Opinion Article

Research Status of CO2 Cured All Solid Waste Cementitious Materials

Abstract: The emission of greenhouse gases such as carbon dioxide CO2 has caused numerous environmental issues. Carbon capture, utilization, and storage (CCUS) technologies serve as critical pathways to directly reduce carbon emissions. Among these, CO2 mineralization curing for building materials is a direct CO2 utilization technology that not only absorbs CO2 but also consumes large amounts of industrial solid waste to produce high-value-added building materials. Since mineralization reactions are spontaneous and require no additional energy input, this method can replace high-energy-consuming traditional autoclave curing processes, reduce production costs, and demonstrate significant market potential. This paper reviews recent research progress on CO2-cured all-solid-waste cementitious materials, focusing on their mechanisms, influencing factors, and performance. The aim is to provide comprehensive references for researchers in related fields and promote further development and application of CO2-cured all-solid-waste cementitious materials.

Keywords: CO2 curing; all-solid-waste; mechanism research; performance research; carbon sequestration

1. Introduction

Global climate issues caused by massive CO2 emissions have intensified, posing urgent challenges to sustainable development [1]. China has proposed to peak CO2 emissions by 2030 and achieve carbon neutrality by 2060 [2]. CO2 mineralization utilizes alkaline mineral components to react with CO2, forming stable carbonates for permanent carbon sequestration. Replacing traditional steam curing in concrete systems with CO2 mineralization is applicable to various concrete products while enhancing strength and durability. Thus, CO2 mineralization is recognized as an effective method for permanent carbon sequestration and carbon neutrality [3]. China produces over 3.3 billion tons of industrial solid waste annually, with accumulated stockpiles exceeding 60 billion tons, including blast furnace slag, steel slag, red mud, non-ferrous metal slag, fly ash, coal slag, sulfuric acid slag, waste gypsum, desulfurization ash, and carbide slag (CS) [4–5]. Unregulated disposal of industrial solid waste not only occupies land but also releases acidic/alkaline inorganic and organic pollutants. Geopolymers, synthesized from aluminosilicate materials under alkaline activation, form amorphous or quasi-crystalline three-dimensional network structures through dissolution, depolymerization, and polycondensation [6]. Geopolymer production consumes only 10% of the energy required for cement, reduces emissions by 90%, and offers advantages such as high durability, impermeability, early strength, and rapid setting [7]. While early geopolymers used metakaolin, recent studies have expanded to blast furnace slag, steel slag, fly ash, desulfurization slag (DS), and carbide slag [8]. Combining all-solid-waste geopolymer production with CO2 mineralization curing can address industrial waste treatment challenges while achieving carbon sequestration [9]. However, research on CO2-cured all-solid-waste geopolymers remains limited, and the impact of CO2 curing on carbon fixation and material performance warrants further investigation. Alkaline components in industrial solid waste (e.g., C3S, C2S, CaO, MgO, Ca(OH)2, and C-S-H) can absorb CO2 to form carbonates, demonstrating excellent CO2 mineralization and sequestration capabilities [10, 11]. CO2 curing refines pore structures, enhances mechanical and durability properties [12–14], and mitigates issues like poor stability and heavy metal leaching in industrial solid waste [15].

2. Mechanisms of Mineralization Curing

CO2 curing technology for concrete has gained recognition in carbon reduction research, but its short development history limits understanding of the process. Due to the complexity of solid-liquid-gas reactions and analytical constraints, many challenges remain unresolved. Studies suggest [16] that low-pressure CO2 curing causes significantly less energy loss (0.013 GJ/m³) compared to traditional steam (0.59 GJ/m³) or autoclave curing (0.71 GJ/m³). CO2-cured concrete exhibits improved impermeability, sulfate resistance, chloride resistance, and frost resistance. Its strength development also surpasses traditional methods, offering clear economic benefits [17]. International applications, such as CO2-cured concrete blocks, have already sequestered 1.5 million tons of CO2 [18]. Current research indicates that CO2 reacts primarily with unhydrated cement particles and calcium silicate hydrates (e.g., Ca(OH)2). Young et al. [19] proposed a two-step mechanism: (1) CO2 dissolves in water to form carbonic acid, and (2) the acid reacts rapidly with calcium silicates to form CaCO3 and calcium silicate hydrate (C-S-H) gel:
Reaction:
nCaO·SiO2 + (n-x)CO2 + yH2O → xCaO·SiO2·yH2O + (n-x)CaCO3

Goodbrack [20] suggested that C-S-H gel is transient, further carbonizing into CaCO3 and silica gel (SiO2·nH2O). Papadakis et al. [21] revised the reaction as:
Reaction:
nCaO·SiO2+ nCO2 + xH2O → SiO2·xH2O + nCaCO3

While CaCO3 has been confirmed via XRD and SEM [19], the existence of silica gel remains unverified. Unlike natural carbonation, accelerated CO2curing often leads to incomplete or uneven reactions due to diffusion limitations [22]. The process involves two stages: rapid surface reactions and diffusion-controlled internal reactions. Key factors include moisture content, CO2 pressure, temperature, and humidity, though the role of CO2 concentration remains debated.

- Influencing Factors of Mineralization Curing

3.1 CO2 Concentration and Pressure

CO2 curing efficiency depends on gas diffusion and transport, influenced by concentration and pressure. Higher CO2 concentration enhances surface penetration, improving curing degree and compressive strength [23]. Ghoshal et al. [24] modeled CO2 absorption and found that higher concentrations accelerate early absorption but have limited impact on final curing. Elevated concentrations also increase CaCO3 crystal size [25]. Higher pressure facilitates CO2 ingress[26], but Shi et al. [27] reported no further improvement beyond 0.2 MPa due to CaCO3 layer formation blocking reactions.

3.2 Pre-Curing

Low water-to-binder ratios improve CO2 curing efficiency, but pre-curing (a dehydration process) is critical[28-30]. Shi et al. [31] identified an optimal residual water-to-binder ratio for maximizing curing degree and strength.

3.3 Post-Wet Curing

CO2-cured concrete with surface CaCO3 layers often exhibits incomplete reactions[27,32-34]. Klemň et al. [35] observed rapid early strength gain under wet curing, comparable to standard curing after 14 days. Shao et al. [29] noted strength improvement in sealed lightweight aggregate concrete despite undetected hydration products. Morshed [36] found increased CaCO3 content and hydrated calcium carboaluminate decomposition during post-wet curing, enabling continued hydration of unreacted cement particles.

4. Conclusion

CO2-cured all-solid-waste cementitious materials offer innovative solutions for industrial waste management and carbon neutrality. This review summarizes the reaction mechanisms, key factors, and performance optimization of CO2 mineralization curing. By converting waste into valuable resources, this technology aligns with industrial solid waste valorization and carbon neutrality goals. With deeper mechanistic insights, technological advancements, and policy support, CO2 curing is poised to drive green transformation in the construction industry, contributing to global climate governance.

References

- Masson-Delmotte V, Zhai P, Pörtner H, et al. IPCC Special Report Global Warming of 1.5 C. Summary for Policymakers[J]. Intergovernmental Panel on Climate Change, 2018.

[2]Ye Y, Yu X Building a Community with a Shared Future for Global Development: A Theoretical Interpretation of General Secretary Xi Jinping's Speech at the 76th United Nations General Assembly General Debate [J]. Teaching and Examination, 2022 (7): 13-15.

[3]SANG S, Yuan L, Liu S, etc Carbon neutral geological technology and its prospects for low-carbon coal application [J]. Journal of Coal Industry, 2022, 47.

[4]WANG W， LIU B Y． Research on green finance support of industrial solid waste treatment industry development in our country[J]． Advances in Environmental Protection，2020，10(4)：521-527．

[5] JIANG X D．Business plan of cement kiln cooperative disposal of industrial solid waste project of SEPA Environmental Protection Company[D]． Shanghai： Donghua University，2015．

[6] LIU Z， ZHOU Y， KONG F L， et al． Study on microstructure and properties of geopolymer based on alkali-activated slag[J]． Bulletin of the Chinese Ceramic Society，2017，36(6)：1830-1834．

[7] ADAM A．Strength and durability properties of alkali activated slag and fly ash-based geopolymer concrete [D]．Melbourne：RMIT University，2009．

[8] DAVIDOVITS J． Geopolymers and geopolymeric materials[J]．Journal of Thermal Analysis，1989，35(2)： 429-441．

[9] NI W， WANG E， ZHOU J． Geopolymers： green cementitious materials in the 21st century[J]． New Material Industry，2003(6)：24-28．

[10] D’ALESSANDRO D M, SMIT B, LONG J R. Carbon Dioxide Capture: Prospects for New Materials[J]. Angewandte Chemie International Edition, 2010, 49(35): 6058-6082.

[11]PAN S Y, CHEN Y H, FAN L S, et al. CO2 mineralization and utilization by alkaline solid wastes for potential carbon reduction[J]. Nature Sustainability, 2020, 3(5): 399-405.

[12]FERNANDEZBERTOS M, SIMONS S, HILLS C, et al. A review of accelerated carbonation technology in the treatment of cement-based materials and sequestration of CO2[J]. Journal of Hazardous Materials, 2004, 112(3): 193-205.

[13]HUANG H, GUO R, WANG T, et al. Carbonation curing for wollastonite-Portland cementitious materials: CO2 sequestration potential and feasibility assessment[J]. Journal of Cleaner Production, 2019, 211: 830-841.

[14]Cao W, Yang Q. Effect of carbonation curing on the durability of carbon fixing steel slag-slaked lime brick[J]. Journal of Building Materials, 2023, 26(3): 324-331.

[15] Li Z. Study on the carbon dioxide fixation mechanism and application of cement-based materials[D]. Wuhan：Wuhan University, 2020.

[16]KASHEF-HAGHIGHI S,GHOSHAL S. CO2 sequestration in concrete through accelerated carbonation curing in a flow-through reactor[J]. Industrial & Engineering ChemistryResearch,2009,49(3):1143- 1149.

[17] MONKMAN S,SHAO Y. Carbonation curing of slag-cement concrete for binding CO2 and improving performance[J]. Journal of Materials in Civil Engineering,2009,22(4):296-304.

[18] EL-HASSAN H, SHAO Y,GHOULEH Z. Effect of initial curing on carbonation of lightweight concrete masonry units[J]. ACI Materials Journal,2013,110(4):441-450.

[19] YOUNG J, BERGER R,BREESE J. Accelerated curing of compacted calcium silicate mortars on exposure to CO2[J]. Journal of the American Ceramic Society,1974,57(9):394-397.

[20] GOODBRAKE C J, YOUNG J F,BERGER R L. Reaction of Beta‐Dicalcium Silicate and Tricalcium Silicate with Carbon Dioxide and Water Vapor[J]. Journal of the American Ceramic

Society,1979,62(3‐4):168-171.

[21] PAPADAKIS V G, VAYENAS C G,FARDIS M N. Fundamental modeling and experimental investigation of concrete carbonation[J]. Materials Journal,1991,88(4):363-373.

[22]BUKOWSKI J,BERGER R L. Reactivity and strength development of CO2 activated non-hydraulic calcium silicates[J]. Cement and Concrete Research,1979,9(1):57-68.

[23] J F Young，R L Berger and J Breese. Accelerated Curing of Compacted Calcium Silicate Mortars on Exposure to CO2. Journal of The American Ceramic Society，1974，57(9):394-397.

[24] Kashef-Haghighi S，Shao Y，Ghoshal S. Mathematical modeling of CO2 uptake by concrete during accelerated carbonation curing[J] . Cem Concr Res，1979，9(79):57.

[25] Bukowski J M，Berger R L. Reactivity and strength development of CO2 activated non-hydraulic calcium silicates[J] . Cem Concr Res，1979，9(79):57.

[26] Zhan B，Poon C，Shi C，CO2 curing for improving the properties of concrete blocks containing recycled aggregates[J] . Cem Concr Compos，2013，42(9):1.

[27] Shi C，Liu M，He P，et al. Factors affecting kinetics of CO2 curing of concrete[J] . J Sustainable Cement-based Mater，2012，1(1):24.

[28] Klemm W A，Berger R L，Accelerated curing of cementitious systems by carbon dioxide: Ⅱ[J] . Cem Concr Res，1972，2(6)：647.

[29] Shao Y，Shi C. Carbonation curing for making concrete products-An old concept and a renewed interest[C] // Proceedings of 6th International Symposium on Cement and Concrete，2006.

[30] Monkmam S，Shao Y. Assessing the carbonation behavior of cementitious materials[J] . J Mater Civil Eng，2014，18(6):768.

[31] Shi C, Zou Q, He F. Kinetic Study on CO~2~ Curing of Concrete [J]. Journal of the Chinese Ceramic Society, 2010, 38(7): 1179.

[32] Shi C，He F，Wu Y. Effect of pre-conditioning on CO2 curing of lightweight concrete blocks mixtures. Construction and Building Materials，2012，26(1):257-267.

[33] Shi C，Wang D，He F，et al. Weathering properties of CO2-cured concrete blocks，Resources，Conservation and Recycling，2012，65:11-17.

[34] Shi C，Liu M，He P，et al. Factors affecting kinetics of CO2 curing of concrete Journal of Sustainable Cement-Based Materials，2012，1(1-2):24-33.

[35] Klemn W A，Berger R L. Accelerated curing of cementitious systems by carbon dioxide:part I. Portland cement. Cement and Concrete Research，1972，2(5):567-576.

[36] Morshed，A . Z. ，Early carbonation curing of fresh concrete and its applications in precast concrete production.