# Opinion Article

# Research Status on Electrochemical Deposition Repair of Concrete Cracks

**Abstract:** Electrochemical deposition repair technology drives ion migration by applying an external electric field, generating insoluble precipitates within cracks to achieve self-healing and matrix strengthening. This technology offers advantages such as strong micro-crack repair capability, environmental friendliness, and high durability. The electrodeposition repair process includes electric field-driven ion migration, nucleation and growth of deposition reactions, and crack filling and interface strengthening. Research shows that electrochemical deposition repair technology can effectively seal cracks, reduce permeability, improve flexural performance, and positively impact concrete desalination and steel reinforcement repassivation. Factors influencing repair effectiveness include electrolyte type, current density, and concrete matrix parameters. Further research is needed in deposition mechanisms, process optimization, and long-term performance.

**Keywords:** Electrochemical Deposition; Concrete Crack Repair; Ion Migration.

1. **Introduction**

Concrete is one of the most widely used building materials in modern civil engineering. However, due to its inherent characteristics and external environmental factors such as load effects, temperature changes, dry-wet cycles, and chemical erosion, concrete structures inevitably develop cracks during service. The presence of cracks not only affects the appearance of concrete structures but also reduces their mechanical performance, accelerating the penetration of harmful substances (e.g. Cl-, O2, and moisture), leading to steel corrosion and seriously threatening the durability and safety of concrete structures. Therefore, timely and effective repair of concrete cracks is of significant engineering importance[1]。Traditional repair methods have certain limitations in repairing alkali-activated concrete cracks, such as poor interface compatibility, low efficiency in micro-crack repair, and difficulty in effectively penetrating micro-cracks due to the porous structure and complex interfaces within concrete, resulting in limited repair effectiveness[2-5]。Thus, researching new and practical methods for repairing concrete cracks is of great practical significance.

**2. Principles of Electrodeposition Repair of Concrete Cracks**

Electrochemical deposition repair technology drives ion migration in an electrolyte solution by applying an external electric field, generating insoluble precipitates（e.g.Mg(OH)2、ZnO、CaCO3），within cracks to achieve self-healing and matrix strengthening. This technology has demonstrated advantages such as strong micro-crack repair capability, environmental friendliness, and high durability in traditional concrete repair.

The typical process of electrodeposition repair of concrete cracks includes:

1. Electric field-driven ion migration: Using concrete as the cathode and an external electrode（e.g.,titanium mesh）as the anode, a direct or pulsed electric field is applied to drive ions such as Mg²⁺、Zn²⁺、Ca²⁺、and OH²⁺in the electrolyte toward the crack region.

（2）Nucleation and growth of deposition reactions: The cathode surface undergoes a reduction reaction,2H2O+2e-→2OH-+H2↑，increasing local pH and promoting the combination of cations and anions to form precipitates such as Mg（OH)2、ZnO or CaCO3.

（3）Crack filling and interface strengthening: Deposits accumulate layer by layer within the crack, forming a dense protective layer that enhances interface bonding with the C-(A)-S-H gel of the concrete matrix through chemical bonding.




Figure 1: Schematic diagram of the principle of electrodeposition repair of concrete cracks

**3. Characterization Indicators and Influencing Factors of Electrochemical Deposition Repair**

**3.1** **Characterization Indicators：**

Electrochemical deposition is a new technology that emerged in the late 20th century for repairing concrete structure damage, particularly suitable for cases where traditional repair techniques are ineffective or costly. This method, widely used in metal materials, has seen active research in China in recent years for protecting metal and alloy materials. The principle of electrochemical deposition was first applied to concrete crack repair by Japanese scholars. In the late 1980s, the Japanese Port and Airport Research Institute and Mitsui Engineering & Shipbuilding Co. proposed the electrochemical deposition repair method for cracks in marine engineering[6]。

Subsequently, Otsuki and Ryu[7]applied this technology to land-based reinforced concrete structures, immersing pre-cracked reinforced concrete specimens in an electrolyte and applying a continuous current for 4-20 weeks. They evaluated the repair effectiveness through weight changes, crack closure, and surface coverage, also measuring water permeability, chloride ion penetration depth, and carbonation depth. The results showed that the deposition layer formed on the concrete surface effectively sealed cracks and formed a coating to prevent harmful component erosion. Initial cracks were typically induced by load, and Ryu[8]evaluated the repair effectiveness of reinforced concrete with shrinkage cracks, immersing specimens with chloride-induced cracks in a ZnSO4 solution for electrochemical repair for 8 weeks. The results indicated that electrochemical deposition repair technology not only sealed concrete cracks and reduced permeability but also positively impacted concrete desalination and steel reinforcement repassivation. Ryu[9]induced cracks in concrete beams through loading, performed repairs, and then conducted flexural performance tests. The results showed that the repaired beams had higher flexural performance than unrepaired specimens. Zhang Qian[10]characterized the repair rate by comparing ultrasonic pulse velocities before and after repair, finding that after 30 days of repair, the repair rates of the specimens reached 26.6%, 32.1%, and 35.0%, respectively.

**3.2** **Influencing Factors:**

Ostuki[7,11]conducted experimental research on the selection of electrodeposition solutions using cement mortar specimens, testing eight solutions:MgCl2、ZnSO4、AgNO3、CuCl2、CuSO4、Ca(OH)2、NaHCO3、Mg(NO3)2The results showed that no deposits formed on specimens in copper chloride, copper sulfate, calcium hydroxide, and sodium bicarbonate solutions; silver deposits formed only around cracks in silver nitrate solution; and more deposits formed on specimens in magnesium chloride, zinc sulfate, and magnesium nitrate solutions.

Domestic research on electrochemical deposition repair technology began in 2004. Jiang Zhengwu[12-14]found that current density significantly affects repair effectiveness. Higher current densities produce larger but loosely arranged and lower-strength deposits, while lower current densities slow deposition but produce denser and higher-strength deposits. Additionally, using porous concrete to represent cracked concrete can effectively evaluate electrochemical repair effectiveness. Chu Hongqiang[15-19]conducted comprehensive research from various angles, including electrolyte type, repair device technical parameters, electrolyte temperature, concrete parameters, and post-repair cement matrix performance changes. He selected ZnSO4、MgSO4、MgCl2、CaCl2、Al2(SO4)3、Pb(NO3)2 solutions for electrochemical deposition experiments, concluding that ZnSO4、MgSO4、MgCl2as electrodeposition solutions, with appropriate experimental devices and parameters, achieve good electrodeposition results. He proposed multiple repair evaluation methods, such as mass increase rate and surface coverage, and found that adding additives to the electrolyte can adjust deposit morphology and deposition speed, inducing smoother and denser deposition layers, thereby reducing surface porosity and improving carbonation resistance. Specimens repaired with MgSO4 showed better carbonation resistance than those repaired with ZnSO4，and grey theory could more accurately predict the carbonation resistance of concrete after electrochemical deposition. Crack repair rates are generally faster in the early stages and slower later, with the rate change pattern independent of electrolyte type. Comparing repair rates under pulsed and direct current showed that pulsed current repair is more effective and can alter deposit morphology.

Li Senlin[20]compared four anode materials: copper-clad niobium platinum wire, platinum-titanium composite wire, platinum-coated titanium wire, and platinum-niobium composite wire. The results showed that the platinum-niobium composite anode had relatively excellent electrochemical performance, minimal loss, and flexibility, making it suitable for bending and setting on different reinforced concrete components. It is an economical and high-performance anode material. Currently, most scholars directly use titanium mesh as the external anode, with limited research on anode material selection and mostly indoor experiments, resulting in relatively little research on anode arrangement methods.

Yao Wu[21] studied the electrochemical deposition repair of concrete cracks from an electrochemical perspective, finding that current density concentrates at the crack tip, with the current density at the crack tip being hundreds of times higher than in adjacent undamaged areas. Li Shichao[22]found that the closer to the cathode, the stronger the electric field, the higher the ion migration efficiency, and the easier the formation of deposits. He also proposed a formula for repair depth as a function of current and electrolyte concentration. Zuo Qingyuan[23]added a surfactant, cetyltrimethylammonium bromide (CTAB), to the electrolyte to improve electrochemical deposition repair effectiveness. With a CTAB content of 2% in ZnSO4 and MgSO4.electrolytes, the results showed that CTAB improved surface coverage, crack healing rate, and permeability coefficient, enhancing the healing effect of electrochemical deposition repair. The composition of deposits in the cracks remained unchanged, but the microstructure became denser than without CTAB. Zeng[24]added CTAB to the electrolyte in the range of 0.25%-2.00% in ZnSO4 and MgSO4.electrolytes. The results showed that with 1.00% CTAB, the bond strength between steel and mortar, chloride ion erosion resistance, and steel corrosion resistance were better after repair. Excessive CTAB weakened the repair effect. Deposit morphology was also affected by CTAB, but the composition remained unchanged.

Chu Hongqiang[19]found that among three water-cement ratios, the mass increase rate and crack healing rate increased with the water-cement ratio, while surface coverage decreased with the water-cement ratio. This may be due to the increased porosity of mortar specimens with higher water-cement ratios. Among three protective layer thicknesses, the mass increase rate, surface coverage, and crack healing rate all decreased with increasing protective layer thickness.

Zhang Qian[10] studied the effects of two conductive materials, carbon nanofibers and carbon black, on the electrochemical deposition repair rate and explored the interaction between these materials and cement concrete. The results showed that both carbon nanofibers and carbon black improved the electrochemical repair rate but reduced compressive strength. The improved repair rate was due to carbon nanofibers acting as micro-scale cathodes during electrochemical repair, enriching deposition sites and increasing the deposition product accumulation rate at cracks. Carbon black significantly reduced the resistivity of cement concrete materials, increasing the deposition rate on the concrete surface.

**4.Conclusion**

Electrochemical deposition repair technology can achieve crack repair, effectively preventing corrosive substances from diffusing into concrete, and can also achieve electrochemical chloride removal, restoring steel reinforcement to a repassivated state. This technology provides an efficient and environmentally friendly solution for concrete crack control, but further research is needed in deposition mechanisms, process optimization, and long-term performance. Future research should integrate materials science, electrochemistry, and artificial intelligence to build a "mechanism-process-performance" integrated research framework, promoting the large-scale application of electrochemical deposition in engineering and supporting the green transformation of civil engineering materials.

**References**

[1]Southeast University, Tianjin University, Tongji University. Principles of Concrete Structure Design.[M].Fifth Edition, China Architecture & Building Press.

[2]Li Jinqi, Xu Wei. Analysis, Repair, and Prevention Measures of Concrete Cracks.[J].China Water Transport (Second Half),2008,8(7):18-188.

[3]Yan Yongdong, Yao Changjian, Liu Ronggui, et al. Research Progress on Durability of Cracked Concrete in Chloride Environments.[J].Journal of Architecture and Civil Engineering,2015,32(04):21-30

[4]Wang Yi, Li Zhenguo, Luo Xingguo. A Brief Review of Concrete Crack Repair Techniques.[J].Concrete,2006(3):91-93.

[5]Yao Jitao, Ma Yongxin, Dong Zhenping, et al. Reliability Appraisal and Strengthening of Buildings: Basic Principles and Methods[M].Beijing Science Press，2003:266-320.

[6]YOKODA M, FUKUTE T. Rehabilitation and protection of marine concrete structure member using electrodeposition method;proceedings of the International RILEM/CSIRO/ACRA Conference on Rehabilitation of Concrete Menber, Melbourne, F, 1992[C].

[7]OTSUKI N, HISADA M, RYU J-S,et al. Rehabilitation of Concrete Cracks by Electrodeposition[J]. Concrete International, 1999, 21(3): 58-63.

[8]J.-S. R. An experimental study on the repair of concrete crack by electrochemical technique[J]. Materials and Structures, 2001, 34: 433-437.

[9]RYOU J S, OTSUKI N. Experimental study on repair of concrete structural members by electrochemical method[J]. Scripta Materialia, 2005, 52(11): 1123-1127.

[10] Zhang Qian. Research on Electrochemical Deposition Repair Technology for Concrete Microcracks[D].University of Jinan,2022.

[11]Otsuki N．Investigation of durability of reinforced concrete member on land repaird by electrodeposition method[J].J Soc Mater Sci2002,51（11）:1278

[12]Jiang Zhengwu, Sun Zhenping, Wang Peiming. Mechanism of Electrochemical Deposition Repair of Reinforced Concrete Cracks[J]. Journal of Tongji University (Natural Science Edition), 2004, 32(11): 1471-1475.

[13]Jiang Zhengwu, Sun Zhenping, Wang Peiming. Repair Effectiveness of Electrochemical Deposition Repair of Reinforced Concrete Cracks[J]. Journal of Southeast University (Natural Science Edition), 2006, 36: 129-134.

[14]Jiang Zhengwu, Xing Feng, Sun Zhenping. Basic Research on Electrochemical Deposition Repair of Reinforced Concrete Cracks[J]. Advances in Science and Technology of Water Resources, 2007, 27(03): 5-8.

[15]Chu Hongqiang. Research on Electrodeposition Technology for Repairing Concrete Cracks[D]. Hohai University, 2005.

[16]Chu Hongqiang, Sun Da, Jiang Linhua. Influence of Electrodeposition Solution Concentration and Temperature on Repairing Concrete Cracks[J].Materials Review, 2010, 24(12).

[17]Chu Hongqiang, Jiang Linhua, Zhang Yan. Prediction of Carbonation Resistance of Concrete After Electrodeposition Treatment Based on Grey Theory[J].Journal of Hohai University (Natural Science Edition), 2010, 38(02): 170-175.

[18]Chu Hongqiang, Jiang Linhua, Xu Yi. Influence of Current Density on Repairing Concrete Cracks by Electrodeposition[J].Journal of Building Materials, 2009, 12(06): 729-733.

[19]Chu Hongqiang, Jiang Linhua, Hua Weibing. Influence of Auxiliary Electrode and Electrode Distance on Deposition Effect[J].Journal of Building Materials, 2005, 8(04): 456-461.

[20]Li Senlin, Lu Qingfa, Xu Ning, Zhang Jun. Research Progress and Directions of Electrodeposition Repair Technology for Concrete Cracks[J].Concrete, 2013, (02): 139-142.

[21]Yao Wu, Zheng Xiaofang. Preliminary Progress in Electrodeposition Repair of Concrete Cracks[J].China Science Foundation, 2005(04): 216-219.

[22]Li Shichao. Experimental Research on Electrochemical Deposition Repair of Reinforced Concrete Cracks[D].Shandong University of Technology, 2014.

[23]Zuo Qingyuan, Chu Hongqiang, Yang Xiaopei, et al. Influence of Cationic Surfactant on Healing Effect of Electrodeposition Repair of Concrete Cracks[J].Concrete, 2020, (03): 33-38.

[24]ZENG Y X, ZUO Q Y, JIANG S, et al. Effect of CTAB on the healing of concrete cracks repaired by electrodeposition and the durability of repaired concrete[J]. Construction and Building Materials, 2022, 326: 126757.