PICT Effects and Anticancer Activity on Rosaniline and Spectral Characterisation of Rosaniline/ Cyclodextrin Covered ZnO/ Nanocrystals

Abstract

Rosaniline/Cyclodextrin covered ZnO nanocrystals are synthesized and characterized by various spectral and microscopic methods. RND molecule exhibits single emission in non-polar and aprotic solvents, whereas in water, α-CD and β-CD dual emission is noticed. Solvent and PM3 studies indicate planar intramolecular charge transfer (PICT) present in RND molecule. Absence of isosbestic point suggest 1:2 or 1:3 inclusion complex is formed.  HOMO-LUMO gap for RND/β-CD inclusion complex was more negative, which support that this complex is more stable than RND/α-CD inclusion complex. Compared to RND/CD inclusion complex, a red or blue shifted absorption and fluorescence maximum was seen in β-CD/RND doped ZnO nanocrystals. Nanoparticle size was measured by TEM-EDS and XRD methods. Molecular docking studies shows, RND have anticancer activity against 2oh4 interacting amino acid residues.

Keywords: Rosaniline, Zinc Oxide nano, Cyclodextrin, Planar Intramolecular Charge Transfer, Inclusion complex, Nanocrystal.

1.  Introduction

In the field of material science, the electron donor–acceptor π-conjugated (D-π-A) compounds have found numerous uses, including dye-sensitized solar cells [1], electrogenerated chemiluminescence materials [2,3], nonlinear optical materials [4] and fluorescence probes [5]. The exceptional optical and electrical capabilities of the D-π-A compounds are largely due to the photoinduced intramolecular charge-transfer (ICT) nature of the excited state [6]. Characterizing the ICT state (i.e., electronic nature and molecular geometry) will provide profound understanding of the connection between molecular structures and attributes.

Zinc oxide nanoparticles are synthesized by several methods such as - high temperature solid–vapor deposition [7], solution phase methods [8], colloidal chemistry techniques [9], sol-gel method [10], phase transfer technique [11], hydrolysis of chelate complex [12] polymer stabilization [13] synthesis in reversed micelles [14], microemulsion [15], alkoxide based process [16] precipitation method [17] spray pyrolysis [18] hydrothermal method [19] laser vaporization condensation [20] and flow injection synthesis [21]. In the present study, the precipitation method has been used for synthesizing ZnO nanoparticles.

In general, ZnO nanoparticles surface area is higher in size and little porosity. Because of the importance of the ZnO nano, in this work aimed to a) analyse the effect of donor–acceptor π-conjugated compound (rosaniline, RND) with cyclodextrin and ZnO nanoparticles, b) investigating the presence of PICT (planar intramolecular charge transfer) in RND; c) synthesizing and characterizing ZnO, ZnO/CD, ZnO/RND, d) studying the impact of doping RND/CD on ZnO nanoparticles, and e) to analyse the anticancer activity of the RND dye.

2.  Experimental

2.1 Preparation of Drug/CD inclusion complex

In a 10 ml standard measuring flask, various quantities of α-CD or β-CD solution (0.1 to 1.0×10-2 M) were taken. The above mentioned flasks were filled with 0.2 ml of the RND stock solution (2×10-2 M). Then the flasks were made up to 10 mL using triple-distilled water. The final concentration of the RND was 4×10-4 M and the experiments were conducted at 298 K.

2.2 Preparation of ZnO and RND/β-CD/ZnO Nanocrystals

100 ml of zinc sulfate (0.01 M) in deionized water was heated for 20 to 30 minutes at 50 to 60 °C. ZnSO4 and 1% NaOH solution (1:2 molar ratio) was vigorously stirred for 12 hours at room temperature. After multiple washings, centrifugation was used to separate the resulting white precipitate [22-27]. Then, the ZnO precipitate was dried for six hours at 100 °C in a hot air oven. The size of the produced ZnO nanocrystals was between 25 and 50 nm.

RND (2×10-3 M) in 20 mL of ethanol, it was progressively added to the CD (1×10-2 M in 80 mL) in deionized water. The aforesaid RND/CD solution was mixed with 100 ml of 0.01 M zinc sulphate. This mixture was heated to 50 °C for an hour using a hot plate with magnetic stirrer. One to two mL of 1% sodium hydroxide were added and vigorously agitated for one to two hours. The aforementioned solution was then frozen and dried at -80 °C (mini-lyophilized). The ZnO/ RND/CD powder sample was gathered and utilized for further investigation.

2.3 Molecular Modeling Studies

Molecular geometry of RND, CD and its inclusion complexes were examined using Spartan 08, a molecular modeling program. The semi-empirical PM3 method in the gas phase and Gaussian 09W software were used to theoretically determine the most stable complexation energy following the structural assembly of two orientation inclusion complexes.

3. Result and Discussion

3.1 Effect of Solvents

The absorption and emission spectra of the rosaniline (4-[(4-aminophenyl) (4-imino-2,5-cyclohexadien-1-ylidene) methyl]-2-methylaniline, RND, Figure 1) were analyzed in various solvent polarities (Table 1, Figure 2). RND have two absorption maxima in all the solvents, but it gives three maxima in water. It's interesting to note that the absorption maximum at 546 nm was seen in water and CD solutions is absent from other solvents. This may be due to the presence of three different aromatic rings (aniline ring, toluidine ring and 4-imino-2,5-cyclohexadien-1-ylidene ring). The absorption spectrum of RND in water is divided into three regions, namely: (i) longer wavelength (LW) absorption bands comprise the region at ~ 546 nm (ii) middle wavelength (MW) band at 336 nm and (iii) shorter wavelength (SW) absorption band at 232 nm. The MW band is ascribed to * transition of the benzenoid system, whereas the LW band can be attributed to * transition within the 4-imino-2,5-cyclohexadien-1-ylidene ring of the RND molecule.

Similar to the absorption maxima, the RND exhibit a high solvent dependence in the excited state suggesting that the electronic state's nature may change, maybe as a result of solvent relaxation in the excited state. In non-polar and aprotic solvents, single emission noticed at 490-500 nm, while in water dual emission noticed shorter wavelength (SW) region at 466 and longer wavelength (LW) region 520 nm. As the solvent's protic character increases, the LW emission becomes more red-shifted. The location of LW band, relative to the MW can be ascribed due to the formation of Planar Intramolecular Charge Transfer (PICT) between the three rings (Figure 3 and Figure 4). PICT is generated in water, ethanol and CD solutions, as evidenced by the emission spectrum shapes that are completely distinct from those of other solvents. The data show that the polarity of the solvents and the kind of substituent had a relative impact on the positions of the bands. The solvents exhibit distinct absorption and emission spectrum shifts, while the CD solution indicates the presence of an RND molecule enclosed within the CD cavity. The presence of PICT/TICT/ICT are already explained in detail [28-38].

To examine the solvent induced PICT changes in the fluorescence spectra of the RND, the emission decay of the normal (466 nm) and PICT emission (520 nm) was measured (Table 1). This analysis together with the normal emission decays is listed in Table 1. This decay behavior indicated the existence of the two different normal emitting species in water which compete with the conformational relaxation times required for the PICT state. The decay time of the slow component is similar to that of PICT emission. This indicates that the equilibrium between the locally excited (LE) state and the PICT state is achieved in water in a rather short period. The decay time of RND in water is similar to α-CD and β-CD solutions.

3.2 Effect of α-CD and β-CD

Absorption and emission spectral maxima of RND was investigated in water, α-CD and β-CD (Table 1, Figure 5). The absorption and emission of RND in water, α-CD and β-CD were appearing at 546, 336, 232 nm and 520, 466 nm respectively. Upon increasing the CD concentrations, no noteworthy spectral changes were noted in RND, however the absorbance slightly raised at the same wavelength whereas, the emission intensity decreased at the same wavelength indicating that RND molecule was entrapped into the CD cavities. The inner side of the CD cavity have non-polar environment and restrict the free rotation of the guest molecule, hence, the absorption and emission intensities of the RND molecule was changed [28-41].  The fluorescence intensity ratio of the PICT band and the normal band were same in the water, α-CD and β-CD solutions; i.e., addition of RND to the CD solution, both the normal and PICT emission bands are equally enhanced. The absorption and emission spectral shifts and shape of RND with α-CD or β-CD is same indicate that both CDs are formed similar type of the inclusion complex.

Since all the three aniline rings size are same, simultaneously RND may form 1:1 or 1:2 (RND:2CD) or 1:3 (RND:3CD) inclusion complex. Formation of 1:1 or 1:2 or 1:3 inclusion complex is indicated by the Benesi-Hildebrand plot of 1/(A-A0) versus 1/[CD] or 1/[CD]2 or 1/[CD]3 and 1/(I-I0) vs. 1/[CD] or 1/[CD]2 or 1/[CD]3. The absence of an isosbestic point in the absorption spectrum support the formation of 1:2 or 1:3 inclusion complex [36-41]. The negative free energy change (ΔG) values (Table 1), reveals that the binding process was spontaneous and thermodynamically stable at the experimental temperature.

3.3 Molecular Modeling

To identify the inclusion process, the ground state geometries of RND, α-CD, and β-CD and their inclusion complexes were optimized using the PM3 technique. Table 2 depicts the various thermodynamic parameters values of the RND, α-CD, β-CD and the inclusion complexes. Compared to isolated RND, α-CD and β-CD significant changes were seen in the polarity of the inclusion complexes.

The height of α-CD and β-CD is 7.8 Å and the interior diameters is ~5.6 and ~6.5 Å, respectively. The horizontal and vertical bond length of RND is 9.65 Å and 8.16 Å respectively (Table 2, Figure 3). Both values are higher than α-CD and β-CD cavity dimensions, hence, RND molecule is partially encapsulated in the CD cavity. Since all the three rings have similar size, any one of the rings oriented toward the CD cavity were the starting points for the optimization process. Compared to RND/α-CD, the ΔE, ΔG, and ΔH values for the RND/β-CD inclusion complexes are more negative. The negative enthalpy and Gibbs free energy show that the complex forms spontaneously and exothermically. The small negative entropy (ΔS) indicates disorder of the system. During molecular recognition and binding, HOMO and LUMO energy gaps for the complexes indicate that the electronic structure of the guest molecules will undergo a significant variation (Figure 3). The RND/β-CD inclusion complex's HOMO-LUMO gap was more negative than that of RND/α-CD inclusion complexes, indicating that the former is more stable. The atoms' electronegative charge is higher than that of other atoms, as indicated by the red color in the molecular electrostatic potential (MEP) image (Figure 3). The stability of the big (EHOMO-ELUMO) values is generally higher. Compared to the inclusion complex, the isolated RND molecule is less stable.

3.4. Effect of doping of RND/ CD on ZnO nanocrystals

The absorption and emission spectra of ZnO, RND/ZnO, β-CD/ZnO and RND/ZnO/β-CD nanocrystals in the solution phase. ZnO nanocrystals exhibit an absorption and an emission band at 320 nm and 420, 355 nm, respectively. Generally, it is understood that the quantity of particles does not directly correlate with the intensity of the absorption and emission, and that the absorption and emission bands are affected by the size, shape, metallic substance, and surrounds of the particles [22-27, 42]. The aforementioned absorption and emission maxima are red shifted to 547, 334, 288 nm, and 400 nm, respectively, when RND is doped on the ZnO nano. When the β-CD solution doped on ZnO nano, the absorbance and emission maxima moved to 250 and 398 nm, respectively. Upon doping of RND/β-CD in to the ZnO nano the absorption and emission maxima red shifted to 340, 239, and 460 nm, respectively. The above absorption and emission spectral changes imply that RND and CD molecules doped and interacted with the ZnO nanoparticles. In general, when the CD or other molecules doped on the nanoparticles, the intensity of tends to rise or decrease and spectral changed noted.

3.5. FE-SEM and TEM images

ZnO nano, RND, β-CD/ZnO and RND/β-CD/ZnO nanomaterials were examined by FE-SEM and EDAX (Figure 6). The morphology of the above materials demonstrate that all are different shapes. ZnO particles form small size balls present in cluster shape; RND present in micro sheet shape; β-CD/ZnO is appear in sheet shape; and RND/β-CD/ZnO present in crystal rock shape image. FE-SEM-EDAX data predicts- (a) ZnO nano contains 57.34 % zinc nano and 42.66 % oxygen, (b) β-CD/ZnO nano comprises 19.67% zinc, 54.42% oxygen and 25.91% carbon, (c) RND contains 73.49 % carbon, 26.51 % nitrogen, and (d) The composition of RND/β-CD/ZnO is 28.29 % zinc, 29.69 % carbon, 38.66 % oxygen and 3.37 % nitrogen. FE-SEM pictures and the atom composition of the nano ZnO, RND are different from RND/β-CD/ZnO conform the formation of new nanomaterials.

TEM images of ZnO, β-CD/ZnO and RND/β-CD/ZnO are displayed in Figure 7. Nano sheet like structures found in the ZnO nanomaterials while nanorod like structure is formed in Β-CD/ZnO. TEM image of ZnO nanosheet were seen to uniformly spherical particles between 20 and 44 nm size and in β-CD/ZnO nano, the particles size between 20 and 40 nm. RND/β-CD/ZnO nano-crystal shape was displayed to be between 20-33 nm. TEM-EDX data supported - (a) ZnO nano contains 69.84 % zinc nano and 30.16 % oxygen, (b) β-CD/ZnO nano comprises 8.79 % zinc, 44.59 % oxygen and 46.61 % carbon, (c)) The composition of RND/β-CD/ZnO is 20.60 % zinc, 26.64 % carbon, 47.08 % oxygen and 5.69 % nitrogen. The presence of ZnO along with RND/β-CD is confirmed by the EDX data for the metallic nanocrystals.

The nanocrystal size is also measured by HR-TEM and X-RD methods. In HR-TEM, the nanocrystal size is measured by IMAGE-J software and average crystal size calculated by origin software. The crystal size is given below: ZnO nano – 24.98 nm, β-CD/ZnO – 23.98 nm, RND/β-CD/ZnO Nano – 19.18 nm. In XRD, Scherer equation is used [D = Kλ/βCosθ]. D = Average particle size, K = constant value (0.94). The crystal size is given below: ZnO nano – 19.30 nm, β-CD – 23.84, RND- 20.17 nm, β-CD/ZnO - 20.69 nm, and RND/β-CD/ZnO Nano – 16.85 nm. Compared to XRD method, 2-3 nm particle size is varied in HR-TEM method.

3.6. Powder X-Ray Diﬀractogram

JCPDS: 03-065-3411 data used to determine the mineral name (3C) and the hexagonal closely packed (HCP) structure. The JCPDS card number 800-075 was used to index all of the diffraction peaks with its standard ZnO face-centered cube peaks. The values of the hkl plane are found at (100), (002), (101), (102), (103), (110), (112) and (201) reflection planes of hexagonal structure of ZnO. Eight diffraction peaks noted in ZnO at 31.80, 34.51, 36.21, 47.52, 56.61, 62.90, 67.91, 69.92 correspond to the reflection planes of hexagonal structure of ZnO. In β-CD, eight peaks observed at 13.39, 19.93, 23.50, 27.65, 31.96, 35.54, 40.58, 48.90 while in β-CD/ZnO ten peaks formed at 10.15, 15.18, 25.41, 28.38, 34.92, 42.29, 49.77, 59.16, 63.32, 70.33. In RND, eight peaks formed at 12.07, 17.05, 19.21, 22.17, 23.39, 27.30, 30.25, 34.31, whereas in RND/β-CD/ZnO eleven peaks formed at 10.30, 12.72, 15.15, 25.40, 28.50, 33.20, 35.50, 42.10, 51.13, 58.95, 62.72. Compared to isolated RND, XRD diffraction patterns of the RND/β-CD/ZnO nanomaterial showed a different form and different peak intensities suggesting that nanocrystals were formed. Further, a number of prominent peaks seen from 10 to 80 degree range supporting the formation of RND/ZnO/β-CD nanocrystal.

3.7. Infrared Spectral Studies

FTIR spectra of ZnO nano, RND, RND/ZnO, β-CD/ZnO and RND/β-CD/ZnO were also measured. Due to the conversion of Zn+2 to ZnO nanoparticles, the ZnO nanocrystals were observed at 3325, 1587, 1450, 592, and 513 cm-1. The frequencies appear at 3325 cm−1 indicate the presence of ZnO and the peak at 592, and 513 cm-1 suggest presence of Zn nanocrystals. It is already reported, the FTIR spectrum of pure ZnO nanocrystals peak appears at 595 cm−1 was the characteristic absorption of ZnO bond and the broad band peak at 3507 cm−1 can be attributed to the characteristic absorption of O-H group. When zinc oxide nano added to β-CD, 3325 cm−1 frequency shifted to 3280 cm−1, while 1587, 1450 cm-1 moved to 1614, 1514 cm-1 and 592, 513 cm-1 peaks shifted to 594, 526 cm-1. The above variation in the FTIR frequencies indicate that ZnO nano particles encapsulated in the CD cavity. In RND, primary and secondary amino group stretching frequency seen at 3338 and 3280 cm-1 respectively, aromatic ring CH stretching frequency appear at 3000 cm-1, aromatic ring stretching frequency observed at 1645 cm-1, and CH3 deformation appears at 1458, 1446, 1274 cm-1. Out of plane bending frequency noticed at 995, 817 cm-1. C-N-C bending frequency appears at 613 cm-1, C-NH2 frequency seen at 2860 cm-1, and CH out of plane bending frequency noticed at 750, 677 cm-1.

When ZnO nano added to RND/β-CD, the above frequencies are shifted to lower or higher wave numbers. In RND/β-CD/ZnO, primary and secondary amino group stretching frequency shifted to 3335 and 3270 cm-1 respectively, the aromatic ring CH and C-NH2 stretching frequency is very weak, aromatic ring stretching frequency moved to 1638 cm-1, and CH3 deformation shifted to 1460, 1270 cm-1. Out of plane bending frequency appear at 1031 cm-1. C-N-C bending frequency moved to 592 cm-1, and CH out of plane bending frequency is also very weak. Compared to RND and β-CD/ZnO, RND/β-CD/ZnO nanomaterials showed a marked change in the frequencies suggesting that the RND/β-CD doped on ZnO nanocrystals.

3.8. DTA Thermogram

DTA profiles of pure ZnO nano, RND, β-CD/ZnO and RND/β-CD/ZnO are also analysed. In ZnO nano, two exothermic and three endothermic peaks were noticed at 226.1, 546.7 °C and 272.6, 731.1 and 919.2 °C. RND exhibits each three exothermic and endothermic peaks at 327.1, 604.8, 871.6 °C and 254.3, 517.3, 660.8 °C. β-CD exhibit one exothermic peak noticed at 128.6 °C. In β-CD/ZnO, two exothermic and four endothermic peaks appear at 224.3, 932.4 °C and 265.2, 354.6, 749.8, 884.1 °C. In β-CD/RND/ZnO, each three endothermic and three exothermic peaks seen at 270.1, 522.8, 945.3 °C, and 217.0, 726.2, 1011.4 °C. The endothermic peaks in the nanomaterials are caused by the loss of water from the CDs. In contrast to the pure RND and ZnO new peak arises in RND/β-CD/ZnO conform the formation of the nanomaterials.

3.9. Molecular Docking

The molecular docking investigation was agreed out in Dassault Systems BIOVIA Discovery Studio v22.1.100, the licensed version. Three-dimensional assembly 3D of our target protein, Epidermal growth factor receptor (EGFR) complex with epiregulin (EREG) was recovered from Protein Data Bank (PDB) https://www.rcsb.org/ (PDB ID:5WB7). Protein preparation involved deleting water molecules, and ions, adding hydrogen atoms, Grid setup was used to find optimal binding positions, and docking was performed.

Molecular docking of RND was given in Fig.7. In the figure 8 A and B shows the 3D and 2D interactions of epidermal growth factor receptor (EGFR) complex with epiregulin (EREG) (PDB ID:5WB7) with RND. The 2OH4 amino acid residues (proteins) interacted with RND was given below: a conventional hydrogen bond seen at Glu915; π- alkyl interaction observed - Leu838, Leu1033, Cys917 and Ala864 and π- π stacked noticed at Phe916. ADMET (Absorption–Distribution–Metabolism–Excretion–Toxicity are the internal processes that describe how a drug moves throughout and is processed by the body) solubility level is 3; ADMET BBB (Blood Brain Barrier is a term used to describe the particular properties of the central nervous system (CNS) vasculature) level is 2; ADMET EXT Hepatotoxic Applicability# MD value is 13.908. ADMET EXT CYP2D6# prediction is false; ADMET EXT Hepatotoxic# prediction is true and ADMET EXT PPB# prediction is also true. The LibDock score is 82.51. The above values revealed RND molecule having anticancer activity against 2OH4 amino acid protein.

4. Conclusion

Rosaniline/CD/ZnO nanocrystals are synthesized and characterized by various spectral and microscopic methods. RND molecule exhibits single emission in non-polar and aprotic solvents, whereas in water, α-CD and β-CD dual emission is noticed. Solvent and PM3 studies suggest PICT present in RND molecule. Absence of isosbestic point suggest 1:2 or 1:3 inclusion complex is formed.  HOMO-LUMO gap for RND/β-CD inclusion complex was more negative, which support that this complex is more stable than RND/α-CD inclusion complex. Compared to RND/CD, a red or blue shifted absorption and fluorescence maximum was seen in RND/β-CD/ZnO nanocrystals. SEM and TEM images confirm the presence of Nanocrystals. Molecular docking studies shows RND molecule having anticancer activity against 2OH4 amino acid protein

Abbreviations

| FTIR | Fourier Transform Infrared Spectroscopy |
| --- | --- |
| DTA | Differential Thermal Analysis |
| XRD | X-ray Diffraction |
| SEM | Scanning Electron Microscopy |
| TEM | Transmission Electron Microscopy |
| HOMO | Highest Occupied Molecular Orbital |
| LUMO | Lowest Unoccupied Molecular Orbital |
| ZnO NPs | Zinc Oxide nanoparticles |
| α-CD | Alpha Cyclodextrin; |
| β-CD | Beta Cyclodextrin |
| RND | Rosaniline |
| PM3 | Parametric Method 3 |
| ΔE | Internal Energy Change |
| ΔH | Enthalpy Change |
| ΔG | Free Energy Change |
| ΔS | Entropy Change |

- Declaration of generative AI in scientific writing

The authors declare during the preparation of this work no AI and AI-assisted technologies used.

References

- [1] Kitamura, T., Ikeda, M., Shigaki, K., Inoue, T., Anderson, N.A., Ai, X., Lian, T., Yanagida, S. Phenyl-Conjugated Oligoene Sensitizers for TiO2 Solar Cells. Chem. Mater. 2004; 16:1806-1812. doi.org/10.1021/cm0349708.

[2] Lai,  R. Y., Kong, X., Jenekhe, S. A., Bard, A. J. Synthesis, Cyclic Voltammetric Studies, and Electrogenerated Chemiluminescence of a New Phenylquinoline-Biphenothiazine Donor—Acceptor Molecule. J. Am. Chem. Soc. 2003; 125: 12631-39. doi.org/10.1021/ja036600q

[3] Chen, C.-Y., Ho, J.-H., Wang, S.-L., Ho, T.-I. Excimer and intramolecular charge transfer chemiluminescence from electrogenerated ion radicals of donor–acceptor stilbenoids. Photochem. Photobiol. Sci. 2003; 2: 1232-36.  doi.org/10.1039/B307331A

[4] Coe, B. J., Harris, J. A., Brunschwig, B. S., Garin, J., Orduna, J., Coles, S. J., Hursthouse, M. B. Contrasting Linear and Quadratic Nonlinear Optical Behavior of Dipolar Pyridinium Chromophores with 4-(Dimethylamino)phenyl or Ruthenium(II) Ammine Electron Donor Groups. J. Am. Chem. Soc. 2004; 126: 10418-427. doi: 10.1021/ja047650d

- [5] Willets, K. A., Callis, P. R., Moerner, W. E. Experimental and Theoretical Investigations of Environmentally Sensitive Single-Molecule Fluorophores. J. Phys. Chem. B., 2004; 108: 10465-73. doi. 10.1021/jp049684d

- [6] Ma, W., Wu, Y., Han, J., Gu, D., Gan, F. Large three-photon absorption and intramolecular charge transfer of the bis-donor fluorene-based molecules. J. Mol. Struct. 2005; 752: 9-13. doi.org/10.1016/j.molstruc.2005.05.025

- [7]  P. X. Gao, C. S. Lao, W. L. Hughes, Z. L. Wang, Three-dimensional interconnected nanowire networks of ZnO. J Chem Phys Lett. 408: (2005) 174-178. doi.org/10.1016/j.cplett.2005.04.024

- [8] Hu, Z., Oskam, G., Lee, R., Penn, I., Pesika, N. Searson, P.C. The influence of anion on the coarsening kinetics of ZnO nanoparticles. Phys. Chem. B 2003; 107: 3124-130. doi. 10.1021/jp020580h

- [9]  Wong, E. M., Bonevich, Searson J. E., P. C. Growth Kinetics of Nanocrystalline ZnO Particles from Colloidal Suspensions. J. Phys. Chem. B 1998; 102: 7770-75.  doi.org/10.1021/jp982397n

- [10] Isao Azumaya, Hiroyuki Kagechika, Yoshihisa Fujiwara, Michiya Itoh, Kentaro Yamaguchi, Koichi Shudo. Twisted intramolecular charge-transfer fluorescence of aromatic amides: conformation of the amide bonds in excited states. J. Am. Chem. Soc. 1991; 113: 2833-38. doi.org/10.1021/ja00008a005

- [11] Hu, Z., Chen, S., Peng, S. Preparation of Nanosize Cu–ZnO/Al2O3 Catalyst for Methanol Synthesis by Phase Transfer with Metal Surfactant: A Study of Preparation Conditions. J. Colloid Interface Sci. 1996; 182: 457-60. doi.org/10.1006/jcis.1996.0487

- [12] Inubushi, Y., Takami, R., Iwasaki, M., Tada, H., Ito, S. Mechanism of Formation of Nanocrystalline ZnO Particles through the Reaction of [Zn(acac)2] with NaOH in EtOH. J. Colloid Interface Sci. 1998; 200: 220-27. doi.org/10.1006/jcis.1997.5354

- [13]  Taubert, A., Glasser, G., Palms, D. Kinetics and Particle Formation Mechanism of Zinc Oxide Particles in Polymer-Controlled Precipitation from Aqueous Solution. Langmuir 2002; 18: 4488-94. doi.org/10.1021/la011799a

- [14] Kaneko, D., Shouji, H., Kawai, T., Kon-No, K. Synthesis of ZnO Particles by Ammonia-Catalyzed Hydrolysis of Zinc Dibutoxide in Nonionic Reversed Micelles. Langmuir, 2000; 16: 4086-89. doi.org/10.1021/la990931s

- [15]  Zou, B.S., Volkov, V. V., Wang, Z. L. Optical Properties of Amorphous ZnO, CdO, and PbO Nanoclusters in Solution. Chem. Mater. 1999; 11: 3037-43. doi.org/10.1021/cm9810990

- [16] Carnes, C.L., Klabunde, K. J. Synthesis, Isolation, and Chemical Reactivity Studies of Nanocrystalline Zinc Oxide. Langmuir 2000; 16: 3764-72. doi.org/10.1021/la991498p

- [17] Rodrguez-Paez, J.E., Caballero, A.C., Villegas, M., Moure, C., Duran, P., Fernandez, J.F. Controlled precipitation methods: formation mechanism of ZnO nanoparticles. J. Eur. Ceram. Soc. 2001; 21: 925-30. doi.org/10.1016/S0955-2219(00)00283-1

- [18]  Zhao, X.Y., Zheng, B. C., Li, C. Z., Gu, H. C. Acetate-derived ZnO ultrafine particles synthesized by spray pyrolysis. Powder Technol. 1998; 100: 20-23. doi.org/10.1016/S0032-5910(98)00047-3

- [19]  Li, W. J., Shi, E. W., Tian, M. Y., Wang, B. G., Zhong, W. Z. The Synthesis of ZnO Acicular Particles by the Hydrothermal Discharging-gas Method. J. Mater. Res. 1999; 14: 1532-37. doi.org/10.1557/JMR.1999.0205

- [20]  Zhang, S.C., Li, X. G. Preparation of ZnO particles by precipitation transformation method and its inherent formation mechanisms. Colloid Surface Physicochem. Eng. Aspect. 2003; 226: 35-44. doi.org/10.1016/S0927-7757(03)00383-2

- [21] El-Shall, M.S., Graiver, D., Pernisz, U., Baraton, M.I. Synthesis and characterization of nanoscale zinc oxide particles: I. laser vaporization/condensation technique. Nano struct. Mater. 1995; 6 : 297-300. doi.org/10.1016/0965-9773(95)00056-9

[22] Surabhi Siva Kumar, Putcha Venkateswarlu, Vanka Ranga Rao, Gollapalli Nageswara Rao, Synthesis, characterization and optical properties of zinc oxide nanoparticles. International Nano Letters, 2013; 3: 30-35. doi.org/10.1186/2228-5326-3-30

[23] Ramasamy, P., Mani, A., Sneha, B., Nivetha, E., Venkatesan, M., Rajendiran, N. Azo-hydrazo tautomerism in Sudan Red-B and Cyclodextrin/ Sudan Red-B doped ZnO nanomaterials, J Molecular Structure, 2025; 1329: 141423- 431. doi.org/10.1016/j.molstruc.2025.141423

[24] Mani, A., Ramasamy, P., Antony Muthu Prabhu, A., Rajendiran, N. Investigation of Ag and Ag/Co bimetallic nanoparticles with naproxen-cyclodextrin inclusion complex. J.Molecular Structure 2023; 1284: 135301-10, doi.org/10.1016/j.molstruc.2023.135301

[25]  Mani, A., Venkatesh, G., Senthilraja, P., Rajendiran, N. Synthesis and Characterisation of Ag-Co-Venlafaxine-Cyclodextrin Nanorods. European J Advanced Chemistry Research, 2024; 5: 9-16. doi; 10.24018/ejchem.2024.5.1.147

[26] Mani, A., Ramasamy, P., Antony Muthu Prabhu, A., Senthilraja, P., Rajendiran, N. Synthesis and Analysis of Ag/Olanzapine /Cyclodextrin and Ag/Co/Olanzapine /Cyclodextrin Inclusion Complex Nanorods. Physics and Chem. Liquids, 2024; 62: 196-209. doi.org/10.1080/00319104.2023.2297223

[27] Mani, A., Ramasamy, P., Antony Muthu Prabhu A., Senthilraja P., Rajendiran, N. Synthesis and Characterisation of Ag/Co/Chloroquine/Cyclodextrin Inclusion Complex Nanomaterials J Sol-Gel Science and Technology, in press 2005; doi.org/10.1007/s10971-024-06620-5.

[28] Rotkiewiecz, K., Grellmann, K. H., Grabowski, Z. R. Reinterpretation of the anomalous fluorescense of pn, n-dimethylamino-benzonitrile. Chem. Phys. Lett. 1973; 19: 315-18. doi.org/10.1016/0009-2614(73)80367-7

[29] Zachariasse, K.A. Comment on “Pseudo-Jahn–Teller and TICT-models: a photophysical comparison of meta-and para-DMABN derivatives” [Chem. Phys. Lett. 305: (1999) 8]: The PICT model for dual fluorescence of aminobenzonitriles. Chem. Phys. Lett. 2000; 320: 8-13. PII: S0009- 2614 00 00230-X

[30] Demeter, A., Druzhinin, S., George, M., Haselbach, E., Roulin, J. L. Zachariasse, K. A. Dual fluorescence and fast intramolecular charge transfer with 4-(diisopropylamino)benzonitrile in alkane solvents. Chem. Phys. Lett. 2000; 323:351-360. doi.org/10.1016/S0009-2614(00)00473-5

[31] Zachariasse, K. A., Druzhinin, S., Bosch, W., Machinek, R. Intramolecular Charge Transfer with the Planarized 4-Aminobenzonitrile 1-tert-Butyl-6-cyano-1,2,3,4-tetrahydroquinoline (NTC6). J. Am. Chem. Soc. 2004; 126: 1705-15. doi.org/10.1021/ja037544w

[32] Cheng Zhong, The driving forces for twisted or planar intramolecular charge transfer. Phy. Chem. Chem. Phy. 2015; 17: 9248-57.  Doi. org/10.1039/C4CP02381A

[33] Nag, A., Dutta, R., Chattopadhyay, N. Bhattacharyya, K. Effect of cyclodextrin cavity size on twisted intramolecular charge transfer emission: Dimethylamino benzonitrile in β-cyclodextrin. Chem. Phys. Lett. 1989; 157: 83-87. doi.org/10.1016/0009-2614(89)87212-4

[34] Cho, D. W., Kim, Y. H,. Kang, S. G., Yoon, M., Kim D. Cyclodextrin effects on intramolecular charge transfer of 2-biphenylcarboxylic acid: a pre-twisted molecule. J. Chem. Soc. Faraday Trans. 1996; 92: 29-33. Doi. org/10.1039/FT9969200029

[35] Kim, Y H., Cho, DW., Yoon, M., Kim, D. Observation of Hydrogen-Bonding Effects on Twisted Intramolecular Charge Transfer of p-(N,N-Diethylamino)benzoic Acid in Aqueous Cyclodextrin Solutions. J. Phys. Chem. 1996; 100: 15670-76. doi.org/10.1021/jp9613652

[36]	Jude Jenita, M., Venkatesh, G., Subramanian, V.K., Rajendiran, N. Twisted Intramolecular Charge Transfer effects on fast violet B and fast blue RR: Effect of HP-α-CD and HP-β-CDs J.Molecular Liquids, 2013; 178: 160-167. doi.org/10.1016/j.molliq.2012.11.033

[37] Rajendiran, N., Mohandoss, T., Thulasidhasan, J. Planar Intramolecular Charge Transfer Effects on Meloxicam and Piroxicam drugs with α- and β-cyclodextrins: Spectral and Molecular Modeling Studies, J Indian Chem. Soc. 2016; 93: 1183-1197

[38] Rajendiran, N., Venkatesh, G., Sankaranarayanan, R.K. Dual fluorescence of omeprazole: Effect of solvents and pH, Physics and Chemistry of Liquids, 2014; 52: 738-750. doi.org/10.1080/00319104.2014.924379

[39] Rajendiran, N. Jude Jenita,M.  Encapsulation of 4-hydroxy-3-methoxy benzoic acid and 4-hydroxy-3,5-dimethoxy benzoic acid by native and modified cyclodextrins. Spectrochimica Acta, A 2015; 136: 1349–1357, doi.org/10.1016/j.saa.2014.09.139

[40] Jude Jenita, M., Thulasidhasan, J., Rajendiran, N. Encapsulation of alkyl parabens with natural and modified α- and β-CDs, J. Inclusion Phenomena and Macrocyclic Chemistry, 2014; 79: 365-381. doi.org/10.1007/s10847-013-0360-8

[41] G.Venkatesh, G., Saravanan, J., Rajendiran, N.  Cyclodextrin covered organic micro rod and micro sheet derived from supramolecular self assembly of 2,4-dihydroxyazobenzene and 4-hydroxyazobenzene inclusion complexes, Bulletin Chemical Society of Japan, 2014; 87: 283-293, doi.org/10.1246/bcsj.20130255

[42] Sukesh Kashiram Tumram, Rajdip Bandyopadhyaya, Zinc oxide nanostructures: Experiments probing their transformation to nanorods Materials Science and Engineering: B, 2023; 296: 116569. doi.org/10.1016/j.mseb.2023.116569.

Table 1. Absorption and fluorescence spectral maxima of RND with different Solvents, α-CD and β-CD.

| Solvents | abs | log  | flu | τ |
| --- | --- | --- | --- | --- |
| Cyclohexane | 323 240 | 3.67 3.55 | 491 | 30 |
| 1,4-Dioxane | 308 234 | 3.62 3.47 | 498 | 31 |
| Ethyl acetate | 323 245 | 3.67 3.32 | 499 | 32 |
| Acetonitrile | 326 239 | 3.52 3.32 | 501 | 32 |
| 2-Propanol | 338 245 | 3.81 3.61 | 515 | 32 |
| Ethanol | 338 238 | 3.75 3.66 | 466 520 | 26 32 |
| Water | 546 336 232 | 3.13 3.81 3.82 | 466 520 | 26 32 |
| α-CD (0.01 M) | 547 337 232 | 3.27 3.95 4.20 | 467 521 | 26 32 |
| β-CD (0.01 M) | 546 336 233 | 3.61 3.94 4.10 | 466 520 | 26 32 |
| α-CD K (1:1) x105 M-1 | 50 | - | 161 |  |
| β-CD K (1:1) x105 M-1 | 95 | - | 109 |  |
| α-CD G (kcalmol-1) | -12.5 | - | -15.7 |  |
| β-CD G (kcalmol-1) | -14.3 | - | -14.7 |  |
| Excitation wavelength (nm) | - | - | 370 |  |

Table 2. Energetic features, thermodynamic parameters and HOMO-LUMO energy calculations for RND and its inclusion complexes by semiempirical PM3 method.

| Properties | RND | α-CD | β-CD | RND/α-CD | RND/β-CD |
| --- | --- | --- | --- | --- | --- |
| EHOMO (eV) | -8.49 | -10.37 | -10.35 | -8.58 | -8.71 |
| ELUMO (eV) | -0.92 | 1.26 | 1.23 | -1.26 | -1.04 |
| EHOMO – ELUMO (eV) | 7.56 | -11.63 | -11.58 | 7.31 | 7.67 |
| Dipole (D) | 6.22 | 11.34 | 12.29 | 9.27 | 14.09 |
| E (kcal mol-1) | -79.65 | -1247.62 | -1457.63 | -1176.72 | -1386.91 |
| ΔE (kcal mol-1) | - | - | - | -8.75 | -150.77 |
| G (kcal mol-1) | -236.50 | -676.37 | -789.52 | -915.29 | -1138.19 |
| ΔG (kcal mol-1) | - | - | - | -2.42 | -112.17 |
| H (kcal mol-1) | -185.54 | -570.84 | -667.55 | -771.64 | -928.91 |
| ΔH (kcal mol-1) | - | - | - | -15.31 | -75.82 |
| S (kcal/mol-Kelvin) | 0.170 | 0.353 | 0.409 | 0.481 | 0.575 |
| ΔS (kcal/mol-Kelvin) | - | - | - | 0.042 | 0.004 |
| ZPE | 221.13 | 635.09 | 740.56 | 857.46 | 962.14 |

kcal/mol; **kcal/mol-Kelvin; ZPE = Zero-point vibration energy

Figure 1. Chemical structure of Rosaniline [RND].

Figure 2. Absorption and fluorescence spectra of RND in different solvents at 303 K: 1) cyclohexane 2) 1,4-dioxane 3) ethyl acetate 4) acetonitrile 5) 2-propanol 6) ethanol 7) water.

(a) PM3 optimized structure for RND

(b) HOMO, LUMO

(c) MEP

Figure 3. PM3 optimized structures of (a) RND (b) HOMO, LUMO and (c) MEP of RND. The green and red colors represent the molecules' positive and negative phases, respectively, while the blue color shows the nitrogen atom.

Figure 4 Donor–Acceptor  (D–A ) type chromophore may twist or flatten in its excited state to form a TICT (twisted intramolecular charge transfer) state or a PICT (planar intramolecular charge transfer) state. FC- Franck Condon state.

Figure 5. Absorption and fluorescence spectra of RND in different α-CD and β-CD concentrations (M): (1) 0, (2) 0.001, (3) 0.002, (4) 0.004, (5) 0.006, (6) 0.008, (7) 0.01. Insert figure: absorbance and fluorescence intensity vs [α-CD] or [β-CD].

Figure 6. SEM images for (a) ZnO, (b) ZnO/β-CD, (c) RND, (d) ZnO/RND/β-CD nanocrystals.

Figure 7. TEM images for (a-c) ZnO, (d-f) ZnO/β-CD, (g-i) ZnO/RND/β-CD.

Figure 8. Molecular Docking of RND- 2OH4 interacting amino acid residues