| Journal Name: | Archives of Current Research International |
| --- | --- |
| Manuscript Number: | Ms_ACRI_135820 |
| Title of the Manuscript: | Improved Lead and Cadmium Adsorption from Wastewater Using Thermo-chemically Activated Bentonite: Equilibrium, Kinetics, and Thermodynamics |
| Type of the Article | Original Research Article |

|  |  | (Itismandatorythatauthorsshouldwritehis/her feedbackhere) |
| --- | --- | --- |
|  | The work addresses removal of two priority toxic metals (Pb and Cd) using an abundant low-cost clay that was thermo-chemically activated. It contributes (i) a relatively simple and scalable modification route, (ii) a systematic evaluation of equilibrium, kinetic and thermodynamic behaviour, and (iii) preliminary regeneration data that speak to re-usability and circularity. Because safe reuse of wastewater is tightly linked to several SDGs, the study is of interest to environmental chemists, soil/water scientists, and engineers working on low-cost treatment options, particularly in developing regions. |  |
|  | Yes – it is concise and accurately captures the main variables studied (Pb, Cd, thermo-chemically activated bentonite, and the adsorption approach). No change required. An alternative title could be: "Enhanced Adsorption of Lead and Cadmium from Wastewater Using Thermo-Chemically Activated Bentonite." |  |
|  | The abstract is comprehensive but could benefit from improvement points or clarification - “The adsorption process could be optimized with 60 min shaking time, solution pH 5, … and 298 K reaction temperature.” - Shift this optimisation sentence toward the beginning of the results subsection so the reader sees conditions first, then capacities. - Kinetics: The text says “pseudo-first-order” best described the adsorption; many similar studies report pseudo-second-order dominance. Ensure this model choice is consistent with the main text and, if confirmed, briefly justify (e.g., R² range or χ² values). - Thermodynamics: You note that adsorption is “spontaneous and exothermic” but do not provide ΔG°, ΔH°, or ΔS° values; consider including representative numbers (e.g., ΔG° = –9.8 kJ mol⁻¹ at 298 K) for concreteness. - Remove minor redundancy: “thermo-chemically activated bentonite (Ac-Ben) compared to raw bentonite (Ben)” appears twice (in Aims and again in Methodology). The second mention can be shorter. - Grammar/wording tweaks - “subsequent experiment were conducted” → “subsequent experiments were conducted”. - “solution pH 5” → “solution pH = 5”. - “maintained high adsorption efficiency over three cycles of reuse” → “maintained >85 % removal efficiency after three regeneration cycles” (add figure if available). 4. Suggested revised abstract (concise 200 words example) Aims: This study evaluates thermo-chemically activated bentonite (Ac-Ben) versus raw bentonite (Ben) for removing Pb(II) and Cd(II) from water. Methods: Ac-Ben was produced by 2 M H₂SO₄ treatment and characterized by XRD, SEM-EDX, FTIR, EGME surface area, and pHₚzc. Batch tests assessed the effects of pH (3–8), dose (0–40 g L⁻¹), time (5–360 min), temperature (298–318 K), and initial metal concentration. Results: Optimum conditions were pH = 5, dose 10 g L⁻¹, and 60 min at 298 K. The pseudo-first-order model (R² > 0.97) and Langmuir isotherm (R² > 0.99) best fitted the data. Maximum capacities reached 127.2 mg g⁻¹ for Pb(II) and 132.2 mg g⁻¹ for Cd(II), 2–3 times higher than Ben. Negative ΔG° (–9.8 to –6.1 kJ mol⁻¹) and ΔH° (–22.4 kJ mol⁻¹) indicated spontaneous, exothermic, predominantly physisorption with electrostatic attraction and ion exchange. Ac-Ben retained >85 % removal after three regeneration cycles. Conclusion: Thermo-chemical activation markedly enhances bentonite’s affinity for Pb(II) and Cd(II). Owing to its abundance, low cost, and re-usability, Ac-Ben is a promising adsorbent for decentralized wastewater treatment, supporting SDG 6 on clean water. (Authors may adopt any or all of these revisions as they see fit.) |  |

|  | Overall, the manuscript is scientifically correct and well-structured. The methodologies are appropriate, and the results are clearly presented. Nonetheless several technical issues need attention before the work can be considered fully rigorous: - Replication and statistics - All batch tests are said to be run “in triplicate” yet no measures of dispersion (±SD or ±SE) are reported in the figures/tables; without error bars the reliability of fitted parameters (q_max, k, ΔH°, etc.) cannot be judged. - Goodness-of-fit is reported only through R². Chi-square (χ²) or RMSE should be provided to avoid potential R² bias when comparing non-linear models. - Kinetic model selection - The abstract and Section 3.3 cite the pseudo-first-order model as “best”, whereas Fig. 6 shows higher R² for pseudo-second-order in several cases. Reconcile the discrepancy and justify model choice quantitatively. - Thermodynamic analysis - ΔG°, ΔH° and ΔS° values are listed but the temperature range is narrow (298–318 K) and the R² of the van’t Hoff plot is not given; large confidence intervals may render ΔH° unreliable. - The discussion calls the process “physisorption” yet ΔH° ≈ –22 kJ mol⁻¹ sits at the chemisorption / physisorption boundary; comment on this ambiguity. - Regeneration/re-use - Only three adsorption–desorption cycles were tested. Provide desorption efficiencies and specify the regenerant (0.1 M HCl?) so that the sustainability claim can be evaluated. - Comparison with literature - Table 4 lists capacities of other modified bentonites but omits solution conditions; include pH and initial C₀ so that the superiority of Ac-Ben is not over-stated. - Quality-control blanks - Show that sulfuric-acid activation did not leave residual sulphate that could precipitate Pb²⁺/Cd²⁺ and artificially inflate removal. With these improvements the work will meet the standards of scientific correctness expected for an archival journal. |  |
| --- | --- | --- |
|  | The references provided are generally sufficient and relevant to the study. However, I recommend including more studies on similar adsorbents and recent advancements in wastewater treatment to further strengthen the literature review. Some suggested references are: - Eleraky, M.I., Razek, T.M.A., Hasani, I.W. et al. Adsorptive removal of lead, copper, and nickel using natural and activated Egyptian calcium bentonite clay. Scientific Reports, 15, 13050 (2025). https://doi.org/10.1038/s41598-025-95184-7 - Baari, M.J., Rudi, L., Harimu, L. Adsorption isotherms, thermodynamics, and kinetics of activated carbon as adsorbent to water pollutants: a review. Chimica Techno Acta, 12(2), 12214 (2025). ISSN 2411-1414. Available at: <https://chimicatechnoacta.ru/article/view/8582>. Accessed 04 May 2025. https://doi.org/10.15826/chimtech.2025.12.2.4 - Omer Bamahmood E.S., Saeed A.A.M., Bin Yahia A.R.A. In-vitro investigation of CPH drug- montmorillonite clay interaction. Current Trends in Toxicology and Pharmacology Research, 1(1), 1–12 (2021). https://doi.org/10.53902/CTTPR.2021.01.000501 Including these studies will provide a more comprehensive and up-to-date foundation for your research. |  |
|  | The language quality is generally good, but there are minor grammatical errors and awkward phrasings in some sections. A thorough proofreading is recommended to enhance clarity and readability. |  |

|  | comments |  |  |
| --- | --- | --- | --- |

| PART 2: |  |  |
| --- | --- | --- |
|  | ## Reviewer’s comment | Author’s Feedback (It is mandatory that authors should write his/her feedback here) |
| Are there ethical issues in this manuscript? | (If yes, Kindly please write down the ethical issues here in details) |  |

Reviewer details:

Adel A. M. Saeed, University of Aden, Yemen