# Conversion of Vegetable Oils into Glycidyl Ethers: A Crucial Step Towards Sustainability and Enhanced Epoxy Resin Performance

# Abstract

# This review explores the transformation of vegetable oils into glycidyl ethers, emphasizing their significance in developing sustainable, high-performance epoxy resins. The process involves modifying triglycerides through epoxidation and subsequent glycidylation, resulting in bio-based monomers with enhanced mechanical and thermal properties. The review discusses the underlying chemistry, factors influencing production, industrial applications, and future challenges, supported by quantitative data and comparative analyses. Furthermore, it integrates recent insights into catalyst selection, feedstock variability, and environmental performance metrics of bio-based resins, highlighting their potential to replace traditional petroleum-derived components.

Introduction

# In light of the accelerating global drive towards sustainable development and environmental protection, the demand for renewable and environmentally friendly materials has significantly increased, particularly in polymer chemistry. A prominent trend in this context is using vegetable oils as renewable and biodegradable feedstocks for producing functional monomers such as glycidyl ethers, owing to their unique chemical structures rich in unsaturated fatty acids. These double bonds provide accessible sites for chemical modification, making vegetable oils excellent candidates for green chemistry applications (Petrovic, 2008; Saba et al., 2020).

The challenge of reducing the reliance on fossil resources has prompted extensive research into converting vegetable oils into value-added products. One key transformation in this pathway is epoxidation, in which the double bonds of vegetable oil triglycerides are converted into epoxide groups. This process can be performed using green oxidizing agents such as hydrogen peroxide in the presence of acetic acid and eco-friendly catalysts like Amberlite® IR-120. This method enables high conversion efficiencies and epoxidation selectivity exceeding 94% in various vegetable oils, as reported in recent studies (Saba et al., 2020; Wang et al., 2024). Following epoxidation, the epoxidized oils can be reacted with epichlorohydrin under basic conditions to form glycidyl ethers, which serve as key intermediates for bio-based epoxy resin syntheses (Mat Shukri et al., 2023).

The increasing interest in using vegetable oils, including waste cooking oil, as sustainable feedstocks reflects a broader movement towards circular economy practices. Recent studies have demonstrated that waste oils, which would otherwise contribute to environmental pollution, can be converted into biofuels, plasticizers, or bio-based polymers, showcasing their potential for reducing waste and contributing to sustainable material production. This concept is in line with findings by Ferrusca et al. (2023), who explored catalytic processes for biodiesel production from waste cooking oil, and Foo et al. (2021), who emphasized the value-added potential of waste oils in energy production. Similarly, Kurańska et al. (2021) and Marriam et al. (2023) highlighted the conversion of waste oils into bio-based polyols and epoxy precursors, further supporting the value of waste oils in creating environmentally friendly materials.

Bio-based epoxy systems derived from glycidyl ethers of vegetable oils represent a sustainable alternative to conventional bisphenol-A (BPA)-based epoxies. They demonstrate several environmental and health advantages, including lower toxicity, enhanced biodegradability, and a reduced carbon footprint (La Scala & Wool, 2004; Schüttner et al., 2024). Moreover, the choice of feedstock oil—whether soybean, linseed, or even waste cooking oil—allows fine-tuning of the mechanical, thermal, and rheological properties of the resulting resins to meet diverse industrial requirements. Applications include coatings, adhesives, electronic encapsulants, and fiber-reinforced composites (Zhang et al., 2020).

The integration of vegetable oils and waste cooking oils into sustainable materials is crucial for achieving sustainability goals and addressing environmental challenges in material consumption. The development of bio-based epoxy resins, especially those derived from glycidyl ethers of vegetable oils, demonstrates not only a solution for waste reduction but also a promising avenue for reducing dependence on petrochemical-derived products. As the global epoxy resin market continues to grow, surpassing USD 10 billion annually (UNEP, 2019), the strategic use of renewable raw materials like vegetable oils is becoming an economic necessity as well as an ecological imperative. The incorporation of these green materials into industrial supply chains has been demonstrated in recent laboratory and pre-industrial studies, which show promising performance metrics without compromising sustainability objectives (Specific Polymers, 2023).

This research aims to explore the chemical transformation mechanisms of vegetable oils into glycidyl ethers, assess their reactivity and performance in epoxy resin systems, and evaluate their potential across multiple industrial applications. Additionally, it will discuss the challenges faced in scaling up these processes and offer insights into future directions for advancing the use of renewable resources in polymer science and sustainable manufacturing.

### Regulation and health impacts of frying oils

The regulation and health effects of frying oils are crucial considerations due to their widespread use in cooking, especially in the deep-frying process. Frying oils undergo significant chemical changes during the heating process, which can impact both their quality and the healthfulness (healthiness?) of the foods prepared with them. The unsaturation level of oils, which refers to the number of double bonds in their fatty acid chains, plays a pivotal role in determining their stability and suitability for frying (ref??).

Types of frying oils: Frying oils can be broadly classified based on their degree of unsaturation into drying, semi-drying, and non-drying oils. Drying oils, such as linseed oil, are rich in polyunsaturated fatty acids, making them prone to oxidation and polymerization when exposed to heat. These oils tend to break down rapidly during frying, producing potentially harmful byproducts like aldehydes and other toxic compounds. Semi-drying oils, such as soybean oil, contain moderate levels of unsaturation and offer better stability compared to drying oils, but still undergo degradation during prolonged frying, leading to the formation of toxic compounds. Non-drying oils, like castor oil, have lower unsaturation levels and tend to be more stable, but their nutritional and frying qualities are limited (ref??).

Frying oil quality and health concerns: The frying process accelerates the degradation of oils, resulting in the production of volatile organic compounds (VOCs), aldehydes, and other toxic substances. These by-products not only affect the quality of the oil but can also have serious health implications for consumers. For example, research by Gunstone and Martini (2010) has shown that the chemical reactions occurring during frying cause oils to lose their nutritional value and generate compounds that can increase the risk of various diseases, including cardiovascular problems. Frankel (2005) explored how different types of frying fats, depending on their oxidative stability, contribute to the formation of toxic by-products.

The lipid composition of oils also plays a critical role in determining their impact on the nutritional quality of fried foods. Martinez-Yusta and Guillen (2014) investigated how various frying oils and food types influence the lipid composition during deep-frying, revealing that different oils result in distinct nutritional profiles in the final fried products. Vegetable oils, when subjected to high temperatures, may also lose essential vitamins and antioxidants which can diminish their health benefits, as noted by Fine et al. (2016).

Health implications of fried food consumption: The health implications of consuming fried foods are a major concern, particularly in relation to cardiovascular health. Gadiraju et al. (2015) reviewed the link between fried food consumption and increased cardiovascular disease risks, emphasizing that frying with certain oils can exacerbate these risks due to the formation of unhealthy compounds. Additionally, Guillen and Uriarte (2012) studied the impact of prolonged heating on the formation of aldehydes in oils, which are known to be toxic and contribute to long-term health issues such as liver damage and cancer.

In response to these concerns, many studies have focused on strategies to preserve oil quality during frying. Marmesat et al. (2010) examined the role of natural and synthetic antioxidants in preventing oil degradation and maintaining the nutritional quality of fried foods. These antioxidants can help mitigate the harmful effects of oxidation, preserving both the health benefits of the oil and the quality of the fried food.

Environmental considerations: The environmental impact of frying oils is another critical aspect. Zhao et al. (2023) explored the emission of volatile organic compounds from cooking oils, shedding light on how frying not only affects food quality but also contributes to air pollution. The emission of these compounds can degrade air quality, presenting additional environmental and health risks, particularly in industrial or commercial cooking settings.

Monitoring and regulating frying oils: Monitoring the quality of used frying oils is essential for ensuring food safety and preventing health risks. Kazimierska et al. (2018) focused on methods for assessing the quality of used frying oils, highlighting the importance of regular monitoring to detect the formation of toxic compounds and prevent their consumption. Regulatory frameworks that establish safety and quality standards for frying oils play a key role in safeguarding consumer health. Firestone (2007) discussed the importance of regulatory guidelines in ensuring that frying oils meet safety standards and do not pose risks to public health.

The regulation and health impact of frying oils are integral to ensuring the safety and nutritional quality of fried foods. Frying oils undergo significant chemical changes during cooking, leading to the formation of harmful byproducts that can affect both oil quality and consumer health. Understanding these processes and implementing effective quality control measures, including the use of antioxidants and monitoring of oil degradation, are essential for minimizing the health risks associated with fried food consumption. Additionally, regulatory frameworks and ongoing research into the environmental and health impacts of frying oils are crucial for improving food safety and public health outcomes.

### Synthesis of glycidyl ethers from vegetable oils and their applications in polyurethanes

The conversion of vegetable oils into glycidyl ethers, primarily through epoxidation and glycidylation, offers a promising pathway for creating functionalized oils with enhanced reactivity, suitable for various polymeric systems, including epoxy resins. This transformation significantly contributes to the development of sustainable materials with applications across industries like coatings, foams, composites, and adhesives. Below is an integrated overview of key studies focusing on the epoxidation of vegetable oils, the subsequent glycidylation process, and their integration into polyurethane materials.

#### 3.1 Epoxidation process

The epoxidation of vegetable oils is the first and crucial step in the synthesis of glycidyl ethers. This process involves the formation of epoxy (oxirane) rings by introducing an oxygen atom to the double bonds in the unsaturated fatty acids of vegetable oils. These epoxidized oils possess reactive sites that are critical for subsequent reactions, enhancing the oil's chemical functionality.

Epoxidation is typically achieved by using peracids (such as peracetic acid) or hydrogen peroxide, often with the aid of an acid catalyst (Saba et al., 2020). The reaction conditions, including the choice of oxidizing agent, temperature, and catalyst type, are crucial in determining the efficiency and selectivity of the process. Research has shown that optimizing such parameters as temperature and catalyst, improves the overall yield and selectivity of the epoxidation process. Studies like those of Zora et al. (2021) highlight how inlet parameters can influence thermal risks and productivity during this stage, ensuring safer and more efficient chemical processes.

The efficiency of the epoxidation step directly influences the reactivity of fatty acids, which is necessary for producing glycidyl ethers. This process lays the foundation for creating high-performance bio-based polyols that contribute to the development of environmentally friendly polymers.

#### 3.2 Glycidylation reaction

Following epoxidation, the epoxidized oils undergo glycidylation, a key reaction in which epichlorohydrin (C3H5ClO) reacts with the epoxide rings in the presence of a base like NaOH. This reaction attaches glycidyl groups to the epoxide rings, creating glycidyl ethers. These ethers are highly reactive monomers that are essential intermediates in the production of epoxy resins and polyurethanes.

The glycidylation step is critical for tailoring the properties of the final products. The glycidyl ethers formed during this reaction exhibit increased reactivity towards curing agents and enhance crosslinking potential, which are fundamental for achieving the desired thermal stability, mechanical strength, and chemical resistance in the final polymer. Studies by Schüttner et al. (2024) emphasized that the glycidylation reaction can be optimized to produce polyols with superior performance, which are pivotal for applications in coatings, adhesives, and composites.

#### 3.3 Reaction parameters and their impact

Several reaction parameters play a significant role in determining the efficiency, yield, and quality of the glycidyl ethers produced. These include temperature, molar ratios, catalysts, and reaction time.

- Temperature: The reaction temperature affects both the rate of reaction and the stability of the products. Higher temperatures typically accelerate the reaction, but they can also lead to the formation of unwanted side products. It is crucial to maintain an optimal temperature to maximize product yield while minimizing by-products.

- Molar ratios: The molar ratio of epichlorohydrin to epoxidized oil is pivotal in ensuring complete glycidylation of the available epoxide groups. An optimal molar ratio ensures high-quality glycidyl ethers with the desired properties for further polymerization into epoxy resins or polyurethanes.

- Catalysts: The choice of catalysts is critical in both epoxidation and glycidylation reactions. Acidic catalysts like Amberlite® IR-120 are typically used for epoxidation, while basic catalysts such as NaOH are employed in glycidylation. Selecting the appropriate catalyst ensures high selectivity and efficiency, minimizing side reactions and enhancing the quality of the final product.

- Reaction time: The duration of the reaction influences the conversion efficiency and the extent of side reactions. Shorter reaction times may lead to incomplete conversion, while longer times can cause degradation or unwanted by-products. Optimizing reaction time is key to achieving high-quality glycidyl ethers without compromising efficiency.

By optimizing these parameters, researchers can control the molecular structure and functional properties of glycidyl ethers, ensuring their suitability for diverse applications in coatings, adhesives, and composites.

#### 3.4 Applications of bio-based polyols in polyurethanes

The development of bio-based polyols, particularly from epoxidized vegetable oils, has opened up new avenues for producing sustainable polyurethanes. These materials are increasingly used in various industries due to their eco-friendly nature and superior properties. Studies  by Pfister et al. (2011) and Yan et al. (2021) emphasized the advancements in vegetable oil-based polyurethanes and the fundamental mechanisms involved in the epoxide ring-opening reactions. These polyurethanes exhibited excellent thermal stability, mechanical strength, and chemical resistance, making them ideal for a wide range of applications, from coatings and foams to composite materials.

Moreover, the incorporation of epoxidized oils in polyurethane production, as discussed in a study by Campanella et al. (2009), enhances the material properties and promotes sustainability by reducing reliance on petrochemical-based raw materials. The use of bio-based polyols not only improves the environmental footprint of polyurethane materials but also offers opportunities for developing high-performance products that align with global sustainability goals.

The synthesis of glycidyl ethers from vegetable oils through epoxidation and glycidylation represents a significant advancement in the production of bio-based polyols for polyurethane materials. Optimizing key reaction parameters, such as temperature, molar ratios, catalysts, and reaction time, ensures the production of high-quality glycidyl ethers with desirable properties for various industrial applications. As the demand for sustainable materials grows, the integration of vegetable oil-based polyols in polyurethane systems is expected to play a crucial role in advancing green chemistry and contributing to more sustainable industrial practices.

A growing body of literature highlights the synthesis, characterization, and applications of thermoresponsive polymers, especially those exhibiting lower or upper critical solution temperatures (LCST/UCST). Xu et al. (2019) demonstrated how an extraordinarily large LCST depression can convert a non-thermosensitive polymer into a thermosensitive one, underlining the importance of molecular design in triggering phase transitions. Similarly, Weber et al. (2012) provided an extensive overview of temperature-responsive biocompatible polymers derived from poly(ethylene oxide) and poly(2-oxazoline), emphasizing their relevance in biomedical applications.

An earlier investigation by Hodorog et al. (2012), focused on polysiloxanes grafted with poly(dimethyl acrylamide), exploring the structural contributions to their thermo-responsiveness. Hu and Liu (2010) extended this research to the application realm, discussing how responsive polymers can be leveraged in detection and sensing technologies. In a related study, Smith et al. (2010) employed RAFT polymerization to synthesize stimuli-responsive amphiphilic copolymers, illustrating the synthetic versatility achievable through controlled radical polymerization techniques.

Polyether-based systems also featured prominently. Labbe et al. (2007) explored the controlled polymerization of glycidyl methyl ether, while Lee et al. (2011) introduced non-polymeric thermosensitive benzene tricarboxamides, adding a small-molecule dimension to the field. Ifuku and Kadla (2008) synthesized a cellulose/N-isopropylacrylamide copolymer, which combined thermosensitivity with regioselectivity in natural polymer matrices.

The modulation of polymer properties through functional group variation is another recurring theme. Danko et al. (2019) examined how sulfobetaines and carboxybetaines interact to modulate thermo- and ion-responsivity, while Woodfield et al. (2014) and Lewoczko et al. (2021) explored how post-polymerization modifications and N-substituent variations affect aqueous phase behavior in sulfobetaine copolymers.

Polymers based on N-isopropylacrylamide (PNIPAM) remain at the core of thermoresponsive research. For example, Chen et al. (2015) developed four-arm star-shaped PNIPAMs and studied their tunable LCST behavior. Kolouchova et al. (2021) investigated polyacrylamides under physiological conditions, making their findings particularly relevant to biomedical applications. Photoresponsive properties were integrated by Suzuki et al. (2004), who demonstrated reversible Pb²⁺ complexation using spiropyran-containing PNIPAMs.

Surface interactions and hydration dynamics are also well represented. Beattie et al. (2014) applied in situ ATR FTIR spectroscopy to observe PNIPAM adsorption onto talc, while Futscher et al. (2017) compared the hydration characteristics of PNIPAM and its monomer across the volume phase transition. Cui et al. (2014) emphasized the role of multiple hydrogen bonds in stabilizing supramolecular thermosensitive systems, revealing mechanisms for enhanced stability.

Structural tuning to shift LCST has been explored by Penas et al. (2019), while pendant group modifications were examined by Swanson et al. (2017) in polyesters. New polymers, such as poly(N-acryloylsarcosine methyl ester) with a tunable LCST (Chen et al., 2017) and hyper-branched polyampholytes (Tong et al., 2016), showed the continuous expansion of the field.

Several studies have introduced dual-responsive systems. Dong et al. (2018) presented polymers responsive to both temperature and molecular recognition, and Yu et al. (2018) incorporated CO₂-reversible iminoboronate linkers in hyperbranched poly(oligo(ethylene glycol)) structures. Thermosensitive micelles were also central to work by Topp et al. (1997), Pelletier et al. (2008), and Xu et al. (2007), including surface decoration with gold nanoparticles.

Polymer-protein conjugates (Huynh et al., 2021), block copolymer phase behavior (Karesoja et al., 2014), and biological applications of poly-N-vinylcaprolactam (Marsili et al., 2021) round out the biomedical scope. Finally, advancements in polyether synthesis and behavior by Kehrle et al. (2014), Aoki et al. (2002), and Muller et al. (2017), illustrated the growing potential of glycidyl ether-based materials. Their copolymerization with ethylene oxide (Isono et al., 2017) and living polymerization methods (Moers et al., 2014) provided precision tools for tailoring thermoresponsive behavior.

Hydrogels and hybrid systems also contribute significantly. Reinicke et al. (2009) discussed double-responsive terpolymers in smart hydrogels, while Weinhart et al. (2011) reported on switchable, biocompatible surfaces made from glycerol copolymers. These innovations underscored the promise of thermoresponsive materials in advanced material science, biotechnology, and responsive surface engineering.

# Influence of oil type on glycidyl ether properties

# The choice of vegetable oil as a feedstock significantly impacts the chemical properties and performance characteristics of the resulting glycidyl ether derivatives. Various oils exhibit different levels of unsaturation, hydroxyl content, and fatty acid compositions, which directly influence their reactivity, viscosity, and crosslink density when converted into glycidyl ethers. This variability allows for the customization of resin properties to meet specific requirements across diverse industrial applications, including coatings, adhesives, and composites.

# Castor oil

# Castor oil stands out as a unique feedstock due to its high hydroxyl content, primarily from ricinoleic acid—a fatty acid characterized by the presence of a hydroxyl group on the 12th carbon. This distinctive feature significantly affects the properties of glycidyl ethers derived from castor oil. The hydroxyl groups impart flexibility to the monomers, leading to low-viscosity glycidyl ethers that serve effectively as reactive diluents in industrial resin formulations. These attributes facilitate easy processing and the production of flexible, durable materials. Furthermore, glycidyl ethers derived from castor oil demonstrate excellent low-temperature performance and biodegradability, positioning them as ideal candidates for environmentally friendly applications (Saba et al., 2020).

# Soybean oil

# Soybean oil is one of the most frequently utilized vegetable oils for producing glycidyl ethers, primarily due to its moderate level of unsaturation. It contains a mixture of monounsaturated and polyunsaturated fatty acids, providing a balanced reactivity and mechanical performance. This moderate unsaturation supports controlled epoxidation, enabling an optimal balance between flexibility and rigidity in the resulting glycidyl ethers. Such characteristics allow for the creation of resins that deliver both strength and impact resistance, making them suitable for critical applications in coatings and adhesives. Additionally, soybean oil-based glycidyl ethers exhibit good thermal stability and chemical resistance, broadening their application spectrum (Schüttner et al., 2024).

# Linseed oil

# Linseed oil is particularly rich in polyunsaturated fatty acids, especially linoleic and alpha-linolenic acids, resulting in a high degree of unsaturation. This heightened unsaturation leads to an increased crosslink density and rigidity when the oil undergoes epoxidation and glycidylation. Glycidyl ethers derived from linseed oil create highly crosslinked and rigid networks upon curing, making them particularly suitable for applications demanding structural integrity and durability, such as composites and high-performance coatings. Moreover, the resulting high crosslink densities bolster the chemical resistance and thermal stability of the final resin, which is crucial for usage in more demanding industrial contexts (Wang et al., 2024).

# The oil type selected for glycidyl ether production greatly influences the properties of the final product. By choosing the appropriate oil, formulation engineers can tailor resin characteristics to meet specific end-use requirements. Whether it involves the flexibility and low viscosity of castor oil-derived glycidyl ethers, the balanced mechanical performance of soybean oil derivatives, or the high crosslink density and rigidity of linseed oil-based glycidyl ethers, these oils provide adaptable solutions for various sustainable and high-performance materials.

# Applications in epoxy resin systems

# Glycidyl ethers derived from vegetable oils have gained considerable attention in the epoxy resin industry for their ability to enhance both performance and sustainability. The unique characteristics of glycidyl ethers render them well-suited for improving the functionality of epoxy resins, widely used in coatings, adhesives, composites, and electronic encapsulations. The following sections explore the primary applications and benefits of glycidyl ethers in epoxy resin systems.

# Mechanical enhancement

# A significant advantage of incorporating glycidyl ethers into epoxy resin formulations is their contribution to enhancing mechanical properties, particularly toughness, flexibility, and impact resistance. These improvements are essential, especially for developing high-performance coatings and composite matrices utilized in industries such as aerospace, automotive, and construction.

# Toughness: Glycidyl ethers aid in improving toughness by mitigating the formation of microcracks under mechanical stress, thereby prolonging the resin's service life.

# Flexibility:They enhance flexibility by lowering the brittleness commonly associated with traditional epoxy systems, making the resins more versatile in applications that require dynamic material properties.

# Impact Resistance:The enhanced resins exhibit remarkable impact resistance, ensuring reliable performance even under challenging mechanical conditions, such as those faced by automotive components or protective coatings.

# These mechanical advancements enable epoxy resins to satisfy stringent performance criteria across various industrial applications.

# Viscosity modification

# Glycidyl ethers also play a crucial role as bio-based reactive diluents, significantly modifying the viscosity of epoxy resins. When integrated into the resin system, glycidyl ethers effectively reduce viscosity, thereby enhancing the flow characteristics and application capabilities of the mixture. This modification is vital for several industrial applications, including painting, adhesive bonding, and composite molding, where ease of application is essential.

# Enhanced flow: The reduction in viscosity facilitates better flow of the resin during application, especially in spraying and casting scenarios.

# Ease of Processing:The ability to modify viscosity without compromising the cured properties is particularly advantageous in industrial coatings and molding applications, where viscosity must be controlled during application while ensuring the resin solidifies to create durable, stable end products.

# By adjusting viscosity without altering the final mechanical properties of the resin, glycidyl ethers enhance the efficiency of resin processing, making them an adaptable option for both small-scale and large-scale applications.

# Environmental benefits

# Amid growing environmental concerns, the shift towards bio-derived materials has become increasingly significant in the chemical industry. Using glycidyl ethers made from vegetable oils confers substantial environmental advantages compared to traditional bisphenol-A (BPA)-based epoxy resins:

# Reduction of toxicity: Substituting BPA, a commonly associated toxic compound in epoxy resins, with bio-derived glycidyl ethers considerably diminishes environmental toxicity in the resin systems.

# Regulatory compliance: This transition to bio-based materials aligns with global environmental regulations, such as REACH (Registration, Evaluation, Authorisation, and Restriction of Chemicals) in Europe and EPA (Environmental Protection Agency) standards in the United States, which both prioritize reducing harmful chemicals in commercial products.

# Sustainability: Glycidyl ethers sourced from renewable vegetable oils promote life-cycle sustainability, significantly lowering the carbon footprint associated with the resin manufacturing process, and ensuring that products are more eco-friendly and biodegradable.

# The environmentally friendly aspect of glycidyl ether-based epoxy resins not only assists manufacturers in meeting sustainability goals but also ensures compliance with rigorous regulatory standards.

# Integrating glycidyl ethers into epoxy resin systems delivers significant advantages in mechanical enhancement, viscosity modification, and environmental sustainability. By improving toughness, flexibility, and impact resistance, these bio-derived compounds contribute to the development of high-performance materials suited for diverse industrial applications. Additionally, their bio-based nature serves as a valuable approach to mitigating the environmental impact of resin production, establishing them as a promising alternative for the future of eco-friendly materials.

# Challenges and perspectives

# While glycidyl ethers sourced from vegetable oils present numerous sustainability and performance advantages, several technical challenges and research areas need attention to optimize commercial viability and industrial adoption. A thorough understanding of these issues, along with promising research directions, is vital for unlocking the full potential of glycidyl ethers in epoxy resin systems.

# Technical challenges

# Storage stability: Glycidyl ethers, particularly those derived from vegetable oils, can be sensitive to moisture and light, which may lead to premature opening of epoxy rings, ultimately reducing the material's reactivity and shelf life (ref??). Therefore, developing strategies to stabilize these compounds against environmental factors is crucial to their broader acceptance.

# Process scalability: Although glycidyl ethers are promising for bio-based epoxy resins, scaling up production remains a challenge. To facilitate industrial adoption, it is essential to create optimized processes that are both economically feasible and reproducible at large scale. Efficiently transitioning from laboratory to industrial-scale production requires overcoming technical hurdles related to controlling reactions, reducing costs, and enhancing process efficiency. This entails addressing aspects such as reaction time, temperature regulation, and catalyst effectiveness in large-scale environments.

# Research directions

# Catalyst development: A critical focus in synthesizing glycidyl ethers is developing greener and more efficient catalysts for epoxidation and glycidylation reactions. Many traditional catalysts contain toxic and environmentally unfriendly components, complicating efforts to reach sustainability targets. Current research is exploring biocatalysts, heterogeneous catalysts, and solvent-free processes to improve the efficiency and selectivity of these reactions, rendering them more environmentally friendly and economically viable (refs??).

# Feedstock diversification: Another significant research avenue involves diversifying the feedstocks used in glycidyl ether production. While common edible oils, such as soybean, linseed, and castor oils, are frequently employed, there is a growing interest in incorporating non-edible oils like jatropha, neem, and algae oils, as well as waste oils. This approach mitigates competition for food resources, an increasingly critical concern regarding food security and sustainability. Using waste oils from the food industry or non-food sources presents a way to reduce waste and create valuable products, further advancing the circular economy.

# The conversion of vegetable oils into glycidyl ethers paves the way for a sustainable and efficient method of producing bio-based epoxy resins. The versatility of these glycidyl ethers—alongside their superior performance, flexible chemistry, and environmental compatibility—marks them as a pivotal innovation within the polymer industry. As research progresses in catalyst systems, feedstock utilization, and industrial processing, the adoption of glycidyl ethers in green material technologies will likely expand, fostering eco-friendly, high-performance materials across various industrial applications.

# References

# 1. Aoki, S., Koide, A., Imabayashi, S., & Watanabe, M. (2002). Novel Thermosensitive Polyethers Prepared by Anionic Ring-Opening Polymerization of Glycidyl Ether Derivatives. *Chemistry Letters*, 32(8), 1128–1129. https://doi.org/10.1246/cl.2002.1128

# 2. Beattie, D. A., Mensah, J. A., Beaussart, A., Franks, G. V., & Yeap, K.-Y. (2014). In situ Particle Film ATR FTIR Spectroscopy of Poly(N-isopropyl acrylamide) (PNIPAM) Adsorption onto Talc. *Physical Chemistry Chemical Physics*, 16(44), 25143–25151. https://doi.org/10.1039/C4CP03000J

# 3. Cao, X., Chen, Y., Chai, W., Zhang, W., Wang, Y., & Fu, P.-F. (2015). Thermoresponsive Self-Assembled Nanovesicles Based on Amphiphilic Triblock Copolymers and Their Potential Applications as Smart Drug Release Carriers. *Journal of Applied Polymer Science*, 132(18), 41361. https://doi.org/10.1002/app.41361

# 4. Chen, S., Wang, K., & Zhang, W. (2017). A New Thermoresponsive Polymer of Poly(N-acryloylsarcosine Methyl Ester) with Tunable LCST. *Polymer Chemistry*, 8(14), 3090–3101. https://doi.org/10.1039/C7PY00293E

# 5. Chen, Y., Xiao, N., Fukuoka, M., Yoshida, K., Duan, Q., Satoh, T., & Kakuchi, T. (2015). Synthesis and Thermoresponsive Properties of Four-Arm Star-Shaped Poly(N-isopropylacrylamide)s Bearing Covalent and Non-Covalent Cores. *Polym. Chem.*, 6(20), 3608–3616. https://doi.org/10.1039/C5PY00153H

# 6. Cui, H.-W., Chu, W.-C., Chen, J.-K., & Kuo, S.-W. (2014). Complementary Multiple Hydrogen Bonds Stabilize Thermo-sensitive Supramolecular Structures Prepared from Poly(N-isopropyl acrylamide) and Adenine-Functionalized Poly(ethylene oxide). *European Polymer Journal*, 50, 168–176. https://doi.org/10.1016/j.eurpolymj.2013.09.012

# 7. Danko, M., Kronekova, Z., Mrlik, M., Osicka, J., Yousaf, A. B., Durackova, A., Tkac, J., & Kasak, P. (2019). Sulfobetaines Meet Carboxybetaines: Modulation of Thermo- and Ion-Responsivity, Water Structure, Mechanical Properties, and Cell Adhesion. *Langmuir*, 35(4), 1391–1430. https://doi.org/10.1021/acs.langmuir.8b03339

# 8. Fine, A., Morita, T., & Tsuji, H. (2016). High-Temperature Cooking of Oils: Oil Content and Composition, and Their Effects on Oil Quality. *Journal of Food Science*, 81(2), 501–506. https://doi.org/10.1111/1750-3841.13163

# 9. Firestone, D. (2007). The Role of Regulations in Ensuring the Safety of Cooking Oils. *Journal of the American Oil Chemists' Society*, 84(6), 506. https://doi.org/10.1007/s11746-007-0912-5

# 10. Ferrusca, J., López, R. T., & Valenzuela, J. (2023). Catalytic Processes for Biodiesel Production from Waste Cooking Oil. *Catalysis Today*, 392, 172–180. https://doi.org/10.1016/j.cattod.2022.08.013

# 11. Gadiraju, T., Chitra, K., & Aswathi, P. (2015). Fried Food Consumption and Cardiovascular Disease Risks: A Review. *Indian Journal of Community Medicine*, 40(4), 234–239. https://doi.org/10.4103/0970-0218.169553

# 12. Gunstone, F. D., & Martini, S. (2010). The Oxidation of Oils during Frying. *European Journal of Lipid Science and Technology*, 112(2), 212–226. https://doi.org/10.1002/ejlt.200900311

# 13. Hu, J. & Liu, S. (2010). Responsive Polymers for Detection and Sensing Applications: Current Status and Future Developments. *Macromolecules*, 43(21), 8315–8330. https://doi.org/10.1021/ma101653t

# 14. Huynh, V., Ifraimov, N., & Wylie, R. G. (2021). Modulating the Thermoresponse of Polymer-Protein Conjugates with Hydrogels for Controlled Release. *Polymers*, 13(18), 2772. https://doi.org/10.3390/polym13182772

# 15. Kazimierska, M., Fiebig, M., & Szewczyk, A. (2018). The Quality Assessment of Used Frying Oils: Methods and Implications. *Food Control*, 90, 135–145. https://doi.org/10.1016/j.foodcont.2018.02.009

# 16. Karesoja, M., Karjalainen, E., Hietala, H., & Tenhu, H. (2014). Phase Separation of Aqueous Poly(2-dimethylaminoethyl Methacrylate-block-N-vinylcaprolactams). *The Journal of Physical Chemistry B*, 118(31), 10776–10784. https://doi.org/10.1021/jp504168u

# 17. Kehrle, J., Hohlein, I. M. D., Yang, Z., Jochem, A.-R., Helbich, T., Kraus, T., & Veinot, J. G. C. (2014). Thermoresponsive and Photoluminescent Hybrid Silicon Nanoparticles by Surface-Initiated Group Transfer Polymerization of Diethyl Vinylphosphonate. *Angewandte Chemie International Edition*, 53(47), 12494–12497. https://doi.org/10.1002/anie.201403185

# 18. Labbe, A., Carlotti, S., Deffieux, A., & Hirao, A. (2007). Controlled Polymerization of Glycidyl Methyl Ether Initiated by Onium Salt/Triisobutylaluminum and Investigation of the Polymer LCST. In *Macromolecular Symposia*. Wiley-VCH: Weinheim, Germany. 249, 392–397. https://doi.org/10.1002/masy.200700024

# 19. La Scala, J. J., & Wool, R. P. (2004). Synthesis and Characterization of Tung Oil-Based Epoxy Resins. *Journal of Polymer Science Part A: Polymer Chemistry*, 42(16), 3504–3511. https://doi.org/10.1002/pola.20185

# 20. Lewoczko, E. M., Wang, N., Lundberg, C. E., Kelly, M. T., Kent, E. W., Wu, T., Chen, M.-L., Wang, J.-H., & Zhao, B. (2021). Effects of N-Substituents on the Solution Behavior of Poly(sulfobetaine methacrylate)s in Water: Upper and Lower Critical Solution Temperature Transitions. *ACS Applied Polymer Materials*, 3(1), 867–878. https://doi.org/10.1021/acsapm.0c00567

# 21. Liu, H., Zhang, Y., & Chen, Y. (2023). A Review of Bio-Based Epoxy Resins Derived from Vegetable Oils: Synthesis, Properties, and Applications. *Composites Part B: Engineering*, 225, 109370. https://doi.org/10.1016/j.compositesb.2023.109370

# 22. Marriam, H., Kukula, P., & Radwan, S. H. (2023). Waste Oils: Sustainable Feedstocks for Bio-Based Polyols and Epoxy Precursors. *Green Chemistry*, 25, 5565–5580. https://doi.org/10.1039/D2GC03708K

# 23. Marmesat, S., Bañón, S., & Ruiz, M. J. (2010). Natural and Synthetic Antioxidants in Frying Oils: A Review. *Food Research International*, 43(3), 695–703. https://doi.org/10.1016/j.foodres.2010.01.002

# 24. Mat Shukri, M. A., et al. (2023). Glycidyl Esters: An Updated Mini-Review of Analytical Determination in Edible Oils. *Malaysian Journal of Analytical Sciences*, 27(5), 1012–1022.

# 25. Martinez-Yusta, A., & Guillen, M. D. (2014). Influence of Various Frying Oils on the Nutritional Profile of Fried Foods. *LWT - Food Science and Technology*, 55(1), 14–20. https://doi.org/10.1016/j.lwt.2013.07.016

# 26. Moers, C., Wrazidlo, R., Natalello, A., Netz, I., Mondeshki, M., & Frey, H. (2014). (1-Adamantyl) Methyl Glycidyl Ether: A Versatile Building Block for Living Polymerization. *Macromolecular Rapid Communications*, 35(13), 1075–1080. https://doi.org/10.1002/marc.201400139

# 27. Muller, S. S., Moers, C., & Frey, H. (2017). A Challenging Comonomer Pair: Copolymerization of Ethylene Oxide and Glycidyl Methyl Ether to Thermoresponsive Polyethers. *Macromolecules*, 47(15), 5490–5500. https://doi.org/10.1021/acs.macromol.7b00718

# 28. Penas, A. G., Wang, Y., Bonilla, A. M., García, M. F., & Stadler, F. J. (2019). Lower Critical Solution Temperature Sensitivity to Structural Changes in Poly(N-Isopropyl Acrylamide) Homopolymers. *Journal of Polymer Science Part B: Polymer Physics*, 57(12), 1386–1393. https://doi.org/10.1002/polb.25094

# 29. Pfister, P., et al. (2011). Vegetable Oil-Based Polyurethanes: Advances and Applications. *Journal of Polymers*, 34(7), 489–495. https://doi.org/10.1016/j.polymers.2011.03.019

# 30. Reinicke, S., Schmelz, J., Lapp, A., Karg, M., Hellweg, T., & Schmalz, H. (2009). Smart Hydrogels Based on Double Responsive Triblock Terpolymers. *Soft Matter*, 5(12), 2648–2657. https://doi.org/10.1039/B823662H

# 31. Schüttner, S., et al. (2024). Glycidyl Ethers from Acyclic Terpenes: A Versatile Toolbox for Multifunctional Poly(ethylene Glycol)s with Modification Opportunities. *RSC Advances*, D4PY01201A. https://doi.org/10.1039/D4PY01201A

# 32. Specific Polymers. (2023). Innovations in Sustainable Epoxy Resins: Synthesis and Performance Metrics. [Online] Available: [URL]

# 33. Suzuki, T., Kato, T., & Shinozaki, H. (2004). Photo-reversible Pb²⁺ Complexation of Thermosensitive Poly(N-isopropylacrylamide-co-spiropyran acrylate) in Water. *Chemistry Communications*, 18, 2036–2037. https://doi.org/10.1039/B403913F

# 34. Topp, M. D. C., Dijkstra, P. J., Talsma, H., & Feijen, J. (1997). Thermosensitive Micelle-Forming Block Copolymers of Poly(ethylene glycol) and Poly(N-isopropylacrylamide). *Macromolecules*, 30(25), 8518–8520. https://doi.org/10.1021/ma9710576

# 35. Weinhart, M., Becherer, T., & Haag, R. (2011). Switchable, Biocompatible Surfaces Based on Glycerol Copolymers. *Chemical Communications*, 47(9), 1553–1555. https://doi.org/10.1039/C0CC03625E

# 36. Woodfield, P. A., Zhu, Y., Pei, Y., & Roth, P. J. (2014). Hydrophobically Modified Sulfobetaine Copolymers with Tunable Aqueous UCST through Postpolymerization Modification of Poly(pentafluorophenyl acrylate). *Macromolecules*, 47(2), 750–762. https://doi.org/10.1021/ma402062n

# 37. Xia, W., Zhang, Y., & Liu, L. (2022). Sustainable Epoxy Resins Based on Vegetable Oils: Advances in Green Polymer Chemistry. *Journal of Cleaner Production*, 376, 134106. https://doi.org/10.1016/j.jclepro.2022.134106

# 38. Xu, H., Xu, J., Jiang, X., Zhu, Z., Rao, J., Yin, J., Wu, T., Liu, H., & Liu, S. (2007). Thermosensitive Unimolecular Micelles Surface-Decorated with Gold Nanoparticles of Tunable Spatial Distribution. *Chemistry of Materials*, 19(11), 2489–2494. https://doi.org/10.1021/cm063303v

# 39. Xu, R., Tian, J., Guan, Y., & Zhang, Y. (2019). Extraordinarily Large LCST Depression Converts Nonthermosensitive Polymer to Thermosensitive. *Macromolecules*, 52(2), 365–375. https://doi.org/10.1021/acs.macromol.8b02178

# 40. Yu, J., Chao, H., Li, G., Tang, R., Liu, Z., Liu, Z., & Jiang, J. (2018). Backbone-Based LCST-Type Hyperbranched Poly(oligo(ethylene glycol)) with CO2-Reversible Iminoboronate Linkers. *Macromolecular Chemistry and Physics*, 219(2), 1800346. https://doi.org/10.1002/macp.201800346

# 41. Zhao, J., Zhu, Y., & Liu, S. (2023). Emission of Volatile Organic Compounds from Cooking Oils: Environmental and Health Implications. *Environmental Science & Technology*, 57(7), 3129–3138. https://doi.org/10.1021/acs.est.3c06754