Experimental Evaluation and RSM Optimization of Bio-Grease from Cottonseed Oil Using Sodium Hydroxide and Bio-Based Additives: Thickener and Antioxidant

Abstract

This study focuses on the optimization of biogrease through the chemical synthesis of cottonseed oil glycerin, using lye sourced from empty palm fruit bunches as an alkali and Moringa oleifera as a natural antioxidant. Moringa oleifera leaf extract was used as a corrosion-inhibiting agent. The glycerin was obtained through a transesterification process. Response Surface Methodology was used to predict the glycerin yield, biogrease’s dropping point, and biochemical oxygen demand (BOD). The optimum glycerin yield of 48.51% was attained under the following parameters: a 3:1 methanol-to-oil ratio, a catalyst concentration of 1.5 wt.%, a reaction temperature of 55°C, and a duration of 60 minutes. The optimum dropping point for the grease samples from palm bunch lye and sodium hydroxide was achieved at 167.77°C and 166.32°C, with corresponding BOD values of 14.94 and 17.67 ppm at lye dosages of 7.71 and 9 wt.%, temperatures of 152.87°C and 160°C, and durations of 4.35 and 3 hours. The model-predicted values revealed an error margin of 1.48% and 2.98%, which is less than the 5% acceptable margin, showing that the developed quadratic models accurately captured the relationships between the dropping point, BOD, and considered parameters, including lye concentration, temperature, and reaction time. The grease produced using palm bunch lye performed better than grease from sodium hydroxide, showing superior biodegradability and model consistency.

Key Words; Optimization, Biolubricant, Waste, Biomass, bio grease, Lye, Glycerin, RSM.

1 INTRODUCTION

The world’s most popular feedstocks for lubricant production are petroleum, coal, or natural gas (Abdullah et al., 201; Ozioko et al., 2012). These synthetic lubricants continue to pose major health risks and environmental degradation problems for humans, as they release harmful pollutants into the environment and are not biodegradable. In recent years, lubricants made from vegetable oils have received substantial interest due to their excellent and widely acknowledged physicochemical qualities. Bio-based lubricants provide various benefits, including high viscosity indices that permit operation across a wide temperature range, superior lubricity, enhanced flash points, biodegradability, and environmental friendliness, among other desired properties. Typically, bio-lubricants are created by transesterification, a process that may be catalyzed using acid, base, or enzymatic catalysts. Optimization is the process of improving something, such as a design, method, or decision, to make it work as efficiently and effectively as possible, according to Merriam-Webster’s definition. This method sometimes incorporates mathematical approaches, such as calculating the maximum or minimum of a function. Optimization plays a critical role in discovering practical solutions to real-world situations. The development of optimization techniques is closely linked to significant progress across multiple fields, including computer science, operations research, numerical analysis, game theory, mathematical economics, control theory, management science, business, medicine, life sciences, and artificial intelligence (Jonah, et al., 2021). The area has emerged from the discovery that many quantitative issues across fields have basic mathematical foundations, offering a unified approach to articulating and solving them using existing optimization techniques.

Stat-Ease Inc. developed Design-Expert, which serves as statistical software for Design of Experiments (DOE). The software enables researchers to conduct various studies, such as comparative testing, screening, characterization, optimization, robust parameter design, mixture designs, and combined designs. The software has the capability to screen for up to 50 different factors through the use of test matrices. Response Surface Methodology (RSM) integrates statistical and mathematical methods to examine and model situations where multiple variables affect a response outcome. The primary purpose of RSM is to maximize the output variable by adjusting independent variables (input factors) (Montgomery, 2001). Each experiment in RSM comprises several levels or values assigned to operational conditions (Jurado-Alameda et al., 2003). This concept is commonly employed in experimental design to maximize efficiency and discover optimal conditions with the fewest trials.

This research studied the evaluation and synthesis of glycerin from cottonseed oil and the production of bio-grease using palm bunch lye and sodium hydroxide. Optimization approaches were employed to find the most efficient way to improve glycerin output, dropping point, and biochemical oxygen demand (BOD) while reducing resource usage. This method targeted the optimization of essential reaction parameters, such as mole ratio, catalyst concentration, reaction time, temperature, and lye dosage. Response Surface Methodology was employed to examine the individual effects of various factors as well as their interactions. Through analysis, we determined the ideal conditions needed to produce both glycerin and bio-grease.

2 MATERIALS AND METHOD

The production of glycerin was carried out by the transesterification method. Initially, 100 g of cottonseed oil was measured into a beaker, warmed to about 55°C using an electric heater, and then transferred into a conical flask. A catalyst solution was made by weighing 1.5 g of sodium hydroxide and dissolving it in the necessary amount of methanol. This was performed using a heated plate and a magnetic stirrer to generate a sodium methoxide solution. The resulting sodium hydroxide-methanol combination was then carefully poured into the hot oil, after which the conical flask was securely capped and placed on a magnetic stirrer. The reaction proceeded at a stirring speed of 250 rpm for 55 minutes. After completion, the mixture was transferred into a separating funnel and left undisturbed for 12 hours, allowing the phases to separate naturally through gravity. This process facilitated the separation of biodiesel from glycerin. Glycerin yield was determined as the ratio of glycerin produced to the initial volume of oil used. The study closely evaluated the interaction effects of key reaction parameters, including the methanol-to-oil molar ratio, catalyst concentration (expressed as a percentage of catalyst-to-oil weight), reaction temperature (°C), and reaction time (minutes) using RSM. The experimental design matrix is presented in Table 1. The glycerin obtained from this process was subsequently used in the production of bio-grease.

For the formulation of biogrease using palm bunch lye and sodium hydroxide, the standard synthesis technique reported by (Huei et al., 2020) was utilized. The grease formulation involved using a thickener palm bunch lye solution at a concentration of 12% (w/v) relative to the total volume of glycerin. The synthesis procedure started by placing 50% of the total glycerin volume into a reaction vessel and heating it to 90°C. Once this temperature was attained, 50% of the palm bunch lye solution was added, followed by vigorous stirring to ensure complete mixing. The temperature was then progressively raised to 160°C to enable full integration of the palm bunch lye solution into the cottonseed oil. At this step, the remaining 50% of glycerin and the remaining thickener were added to the mixture, with continuous stirring. The reaction mixture was agitated vigorously for three hours at 160°C to promote grease production. Subsequently, the temperature was progressively lowered to room temperature, resulting in the transformation of the fluid glycerin into a semi-solid grease (Awoyale, et al., 2011; Jiabao, 2015). During the grease formulation, 1 g of Moringa oleifera extract was added as an ingredient. The effects of key process variables, including palm bunch lye dosage (4 wt%, 8 wt%, 12 wt%, 16 wt%, and 20 wt%), reaction temperature (140°C, 150°C, 160°C, 170°C, and 180°C), and mixing time (1 hour, 2 hours, 3 hours, 4 hours, and 5 hours), on the dropping point of the resulting grease were systematically investigated. The experimental design matrices are shown in Table 2 and 3.

Response Surface Methodology (RSM) served as the statistical tool for analyzing data from glycerol extraction and grease production processes. Design-Expert software (version 11 from Stat-Ease Inc., Minneapolis, MN, USA) was used to generate the quadratic polynomial model. The study utilized multiple regression analysis to determine how the response variable related to independent variables while computing the polynomial equation coefficients. Statistical significance testing, along with Analysis of Variance (ANOVA), was used to evaluate the model’s accuracy and reliability. Below, we present the developed quadratic response model, which has been fitted through analysis.

Y= b0+ i=1kbixi+ i=1kbiixi2+ i<jkbijxixj+e   	      Equation (1)

Where:

- YY represents the response variable (sesame biodiesel yield),

- b0b_0 is the intercept value,

- bib_i (i=1,2,…,ki = 1, 2, \dots, k) denotes the first-order model coefficients,

- bijb_{ij} represents the interaction effects between the independent variables,

- biib_{ii} corresponds to the quadratic coefficients of XiX_i, and

- ee is the random error term.

DIFFIT=ỷi-ỷi(i) 					 	     Equation (2)

where ỷi y ^ i and ỷi(i)  y ^ i ( i ) are the regression's forecast for point I both with and without point I.

The difference in fits (DFFITS) was determined to ascertain how influential a point is in a linear regression. Statistically, DFFITS is the studentized form of DFFIT. It is calculated by dividing the DFFIT value by the estimated standard deviation of the fitted value at that specific data point, as shown in Equation 2.2:

DIFFITS = DIFFITSi hii						   Equation (3)

where s ( i ) Si is the standard error estimated without the point in question, and h i i hii is the leverage for the point.

Also, DFFITS is equal to the products of the externally studentized residual (ti(i)) and the leverage factor (hii1 - hii) h i i / ( 1 − h i i )

DFFITS = tiihii1 - hii						    Equation (4)

The RSM optimization process for the grease involved the following: design of experiment, performing the laboratory experiment in accordance with the design matrix, analyses of the results (ANOVA, modelling, graphical analysis (diagnostic analysis and 3-D plots), optimization and validation of results). On the diagnostic analysis, difference in fit (DFFIT) was determined. It is the variation in a point's expected value that results from excluding that point from the regression Table 2 and 3 shows the experimental design matrices for grease produced using palm bunch lye and Sodium hydroxide as thickeners.

Table 1. Experimental design matrix for obtaining glycerin from transesterification process (Akinpelu, et al., 2021).

| Std | Run | A: Methanol /oil ratio | B: Catalyst dosage (wt%) | C: Temperature (0C) | D: Time (minutes) | Glycerin yield % |
| --- | --- | --- | --- | --- | --- | --- |
| 24 | 1 | 3 | 1.5 | 55 | 80 |  |
| 11 | 2 | 1 | 2.5 | 45 | 80 |  |
| 7 | 3 | 1 | 2.5 | 65 | 40 |  |
| 6 | 4 | 5 | 0.5 | 65 | 40 |  |
| 29 | 5 | 3 | 1.5 | 55 | 60 |  |
| 21 | 6 | 3 | 1.5 | 45 | 60 |  |
| 22 | 7 | 3 | 1.5 | 65 | 60 |  |
| 8 | 8 | 5 | 2.5 | 65 | 40 |  |
| 28 | 9 | 3 | 1.5 | 55 | 60 |  |
| 12 | 10 | 5 | 2.5 | 45 | 80 |  |
| 18 | 11 | 5 | 1.5 | 55 | 60 |  |
| 17 | 12 | 1 | 1.5 | 55 | 60 |  |
| 14 | 13 | 5 | 0.5 | 65 | 80 |  |
| 15 | 14 | 1 | 2.5 | 65 | 80 |  |
| 4 | 15 | 5 | 2.5 | 45 | 40 |  |
| 3 | 16 | 1 | 2.5 | 45 | 40 |  |
| 26 | 17 | 3 | 1.5 | 55 | 60 |  |
| 16 | 18 | 5 | 2.5 | 65 | 80 |  |
| 20 | 19 | 3 | 2.5 | 55 | 60 |  |
| 23 | 20 | 3 | 1.5 | 55 | 40 |  |
| 9 | 21 | 1 | 0.5 | 45 | 80 |  |
| 25 | 22 | 3 | 1.5 | 55 | 60 |  |
| 1 | 23 | 1 | 0.5 | 45 | 40 |  |
| 27 | 24 | 3 | 1.5 | 55 | 60 |  |
| 13 | 25 | 1 | 0.5 | 65 | 80 |  |
| 30 | 26 | 3 | 1.5 | 55 | 60 |  |
| 19 | 27 | 3 | 0.5 | 55 | 60 |  |
| 2 | 28 | 5 | 0.5 | 45 | 40 |  |
| 10 | 29 | 5 | 0.5 | 45 | 80 |  |
| 5 | 30 | 1 | 0.5 | 65 | 40 |  |

Table 2. Experimental design matrix for grease production using palm bunch lye.

| Std | Run | A: Lye dosage wt% | B: Temperature (0C) | C: Time (hr) | Dropping point (0C) | BOD ppm |
| --- | --- | --- | --- | --- | --- | --- |
| 4 | 1 | 15 | 180 | 1 |  |  |
| 6 | 2 | 15 | 140 | 5 |  |  |
| 8 | 3 | 15 | 180 | 5 |  |  |
| 17 | 4 | 9 | 160 | 3 |  |  |
| 2 | 5 | 15 | 140 | 1 |  |  |
| 14 | 6 | 9 | 160 | 5 |  |  |
| 5 | 7 | 3 | 140 | 5 |  |  |
| 13 | 8 | 9 | 160 | 1 |  |  |
| 7 | 9 | 3 | 180 | 5 |  |  |
| 18 | 10 | 9 | 160 | 3 |  |  |
| 11 | 11 | 9 | 140 | 3 |  |  |
| 20 | 12 | 9 | 160 | 3 |  |  |
| 9 | 13 | 3 | 160 | 3 |  |  |
| 10 | 14 | 15 | 160 | 3 |  |  |
| 12 | 15 | 9 | 180 | 3 |  |  |
| 19 | 16 | 9 | 160 | 3 |  |  |
| 3 | 17 | 3 | 180 | 1 |  |  |
| 16 | 18 | 9 | 160 | 3 |  |  |
| 15 | 19 | 9 | 160 | 3 |  |  |
| 1 | 20 | 3 | 140 | 1 |  |  |

Table 3. Experimental design matrix for grease production using NaOH as Thickener

| Std | Run | A: NaOH dosage wt% | B: Temperature (0C) | C: Time (hr) | Dropping point (0C) | BOD Ppm |
| --- | --- | --- | --- | --- | --- | --- |
| 4 | 1 | 15 | 180 | 1 |  |  |
| 6 | 2 | 15 | 140 | 5 |  |  |
| 8 | 3 | 15 | 180 | 5 |  |  |
| 17 | 4 | 9 | 160 | 3 |  |  |
| 2 | 5 | 15 | 140 | 1 |  |  |
| 14 | 6 | 9 | 160 | 5 |  |  |
| 5 | 7 | 3 | 140 | 5 |  |  |
| 13 | 8 | 9 | 160 | 1 |  |  |
| 7 | 9 | 3 | 180 | 5 |  |  |
| 18 | 10 | 9 | 160 | 3 |  |  |
| 11 | 11 | 9 | 140 | 3 |  |  |
| 20 | 12 | 9 | 160 | 3 |  |  |
| 9 | 13 | 3 | 160 | 3 |  |  |
| 10 | 14 | 15 | 160 | 3 |  |  |
| 12 | 15 | 9 | 180 | 3 |  |  |
| 19 | 16 | 9 | 160 | 3 |  |  |
| 3 | 17 | 3 | 180 | 1 |  |  |
| 16 | 18 | 9 | 160 | 3 |  |  |
| 15 | 19 | 9 | 160 | 3 |  |  |
| 1 | 20 | 3 | 140 | 1 |  |  |

3 RESULTS AND DISCUSSIONS

3.1 Model fit summary and ANOVA of glycerin yield

Improving the process impacts of the factors on glycerin yield, four alternative models were examined. Among all, the quadratic model was found as the best match. ANOVA findings were examined to create the quadratic model for glycerin production and estimate the ideal reaction conditions. The quadratic equation indicating glycerin production from the transesterification of cottonseed oil, is presented in Equation 5.

Glycerol yield= +48.51 + 2.95A+ 2.25B + 0.8367C + 1.53D + 0.9394AB + 0.7656AD + 0.4119BD -3.07A2- 3.88B2-1.28C2-1.79D2			Equation (5)

Table 4 shows the experimental result for glycerin yield from transesterification of cotton seed oil.  The table revealed how the process factors interacted to affect the glycerin yield. It forms the basis for the optimization process (Alamu, et al., 2007; Onukwuli, et al., 2016; Omotioma, 2021). The results were analysed in Table 5.

Table 4.  Experimental results for glycerin yield from transesterification of cotton seed oil.

| Std | Run | A: Methanol /oil ratio | B:Catalyst dosage (wt%) | C: Temperature (0C) | D: Time (minutes) | Glycerin yield % |
| --- | --- | --- | --- | --- | --- | --- |
| 24 | 1 | 3 | 1.5 | 55 | 80 | 49.01 |
| 11 | 2 | 1 | 2.5 | 45 | 80 | 36.72 |
| 7 | 3 | 1 | 2.5 | 65 | 40 | 35.94 |
| 6 | 4 | 5 | 0.5 | 65 | 40 | 38.58 |
| 29 | 5 | 3 | 1.5 | 55 | 60 | 48.75 |
| 21 | 6 | 3 | 1.5 | 45 | 60 | 45.98 |
| 22 | 7 | 3 | 1.5 | 65 | 60 | 47.99 |
| 8 | 8 | 5 | 2.5 | 65 | 40 | 42.64 |
| 28 | 9 | 3 | 1.5 | 55 | 60 | 48.75 |
| 12 | 10 | 5 | 2.5 | 45 | 80 | 46.53 |
| 18 | 11 | 5 | 1.5 | 55 | 60 | 47.51 |
| 17 | 12 | 1 | 1.5 | 55 | 60 | 42.87 |
| 14 | 13 | 5 | 0.5 | 65 | 80 | 41.13 |
| 15 | 14 | 1 | 2.5 | 65 | 80 | 38.63 |
| 4 | 15 | 5 | 2.5 | 45 | 40 | 41.33 |
| 3 | 16 | 1 | 2.5 | 45 | 40 | 35.44 |
| 26 | 17 | 3 | 1.5 | 55 | 60 | 48.75 |
| 16 | 18 | 5 | 2.5 | 65 | 80 | 48.01 |
| 20 | 19 | 3 | 2.5 | 55 | 60 | 47.63 |
| 23 | 20 | 3 | 1.5 | 55 | 40 | 43.94 |
| 9 | 21 | 1 | 0.5 | 45 | 80 | 33.99 |
| 25 | 22 | 3 | 1.5 | 55 | 60 | 48.75 |
| 1 | 23 | 1 | 0.5 | 45 | 40 | 33.42 |
| 27 | 24 | 3 | 1.5 | 55 | 60 | 48.75 |
| 13 | 25 | 1 | 0.5 | 65 | 80 | 35.19 |
| 30 | 26 | 3 | 1.5 | 55 | 60 | 48.75 |
| 19 | 27 | 3 | 0.5 | 55 | 60 | 41.14 |
| 2 | 28 | 5 | 0.5 | 45 | 40 | 35.00 |
| 10 | 29 | 5 | 0.5 | 45 | 80 | 39.25 |
| 5 | 30 | 1 | 0.5 | 65 | 40 | 34.61 |

To ensure a strong model fit, an ANOVA was performed to examine the individual model coefficients and test for lack of fit. The lack of fit test checks if the model fails to accurately represent the data beyond what can be explained by random error (Tabrizi et al., 2011). The significance of the process variables was evaluated using the F-value and P-value (also known as "prob > F"). A higher F-value and a lower P-value indicate that a model term is more significant (Tabrizi et al., 2011). The results from the second-order response surface model for glycerin yield, presented in Table 5, show an F-value of 121.41 and a P-value of <0.0001, confirming that the model is highly significant. This means the chance of such a high F-value occurring due to random variation is only 0.01%, underscoring the model’s reliability. Model terms with P-values < 0.0500 are considered statistically significant. In this case, the factors A, B, C, D, AB, AD, BD, A², B², C², and D² were identified as key contributors to the model. Furthermore, the Predicted R² value of 0.9556 strongly correlates with the Adjusted R² value of 0.9831 with a difference of less than 0.2 suggesting good model accuracy (Ezeugo, et al., 2024)

Table 5. ANOVA for quadratic model of glycerin yield from cotton seed oil.

| Source | Sum of Squares | df | Mean Square | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 910.31 | 14 | 65.02 | 121.41 | < 0.0001 | significant |
| A-Methanol/oil ratio | 157.06 | 1 | 157.06 | 293.27 | < 0.0001 |  |
| B-Catalyst dosage | 91.40 | 1 | 91.40 | 170.66 | < 0.0001 |  |
| C-Temperature | 12.60 | 1 | 12.60 | 23.53 | 0.0002 |  |
| D-Time | 42.20 | 1 | 42.20 | 78.79 | < 0.0001 |  |
| AB | 14.12 | 1 | 14.12 | 26.36 | 0.0001 |  |
| AC | 0.7439 | 1 | 0.7439 | 1.39 | 0.2569 |  |
| AD | 9.38 | 1 | 9.38 | 17.51 | 0.0008 |  |
| BC | 0.4389 | 1 | 0.4389 | 0.8196 | 0.3796 |  |
| BD | 2.71 | 1 | 2.71 | 5.07 | 0.0398 |  |
| CD | 0.0008 | 1 | 0.0008 | 0.0014 | 0.9705 |  |
| A² | 24.44 | 1 | 24.44 | 45.64 | < 0.0001 |  |
| B² | 38.93 | 1 | 38.93 | 72.70 | < 0.0001 |  |
| C² | 4.22 | 1 | 4.22 | 7.88 | 0.0133 |  |
| D² | 8.27 | 1 | 8.27 | 15.44 | 0.0013 |  |
| Residual | 8.03 | 15 | 0.5355 |  |  |  |
| Lack of Fit | 8.03 | 10 | 0.8033 |  |  |  |
| Pure Error | 0.0000 | 5 | 0.0000 |  |  |  |
| Cor Total | 918.35 | 29 |  |  |  |  |
| Std. Dev. | 0.7318 |  | R² |  | 0.9913 |  |
| Mean | 42.50 |  | Adjusted R² |  | 0.9831 |  |
| C.V. % | 1.72 |  | Predicted R² |  | 0.9556 |  |
|  |  |  | Adeq Precision |  | 29.8098 |  |

3.1.1 Diagnostic reports of the RSM results of the glycerin yield.

### Figure 1, shows the Predicted verses Actual of the glycerin yield from cotton seed oil. The figure reveal the Axes: X-axis (Actual): The experimentally measured values of glycerin yield. Y-axis (Predicted): The glycerin yield values predicted by the RSM model, based on the fitted polynomial equation. The glycerin yield range of the glycerin yield were: 33.42 and 49.01. the consistent alignment across the range shows that the model performs well for both low and high glycerin yield values. Most data points were seen to cluster tightly around the line of best fit, showing a significant correlation between the predicted and actual values (Dumancas et al., 2016; Leung et al., 2006; Fan et al., 2011; Eevera et al., 2009). This implies that the Response Surface Methodology (RSM) model gives an accurate estimate of glycerin production. Table 6 demonstrates the interaction impacts of the process factors and the validation of RSM data for glycerin yield. The findings demonstrate the proximity of the optimal (predicted) glycerin yield to the experimentally achieved yield. The percentage variation between the predicted and experimental values was confirmed to be less than 5%, demonstrating the correctness of the model. Based on this small variation, the RSM findings were successfully confirmed, proving the model's usefulness in maximizing glycerin production.

### Figure 1. Parity plot of predicted versus actual for glycerin yield.

Table 6. Validation of optimum result of the glycerin yield from cotton seed oil.

| Methanol /oil ratio | Catalyst dosage (wt%) | Temperature (0C) | Time (minutes) | Predicted glycerin yield % | Experimental glycerin yield % | Percentage deviation % |
| --- | --- | --- | --- | --- | --- | --- |
| 3 | 1.5 | 55 | 60 | 48.51 | 49.12 | 1.24 |

3.2 RSM result, Model fit summary and ANOVA for the dropping point and BOD of the produced grease from palm bunch lye and NaOH.

In order to optimize the interactive effects of the variables on the dropping points and BOD of the produced grease.  Out of the four models considered, quadratic model was suggested as the most fitted model. Data of the ANOVA was studied to determine the quadratic model for the dropping points and BOD of the produced grease and its optimum reaction conditions. A quadratic equation model of dropping points and BOD for the produced grease using palm bunch lye and Sodium hydroxide in terms of coded factors are presented in Equations 6 – 9.

Dropping point = +169.01 +7.39A -2.13B +5.96C -1.77AB -1.16AC -2.86	BC -16.04A² -5.30B² -8.22C²   								Equation (6)

Dropping point = +166.32 +7.39A -2.12B +5.97C -1.78AB -1.17AC -2.87	BC -16.02A² -5.26B² -8.20C²  								Equation (7)

BOD	= +14.26 – 1.30A +0.7850B -0.3490C -0.1938AB -0.2562AC -0.0462BC +1.21A2 +0.5214B2 +1.69C2 							Equation (8)

BOD = +17.67 -1.30A +0.7830B -0.3480C -0.1962AB -0.2537AC -0.0437	BC+1.21A² +0.5241B² +1.70C²							Equation (9)

Table: 7 and 8 shows the experimental result for the dropping points and BOD for the produced grease. The table revealed how the process factors interacted to affect the dropping points and BOD for the produced grease. It forms the basis for the optimization process (Jiabao,2015).

Table 7. RSM results for grease produced using palm bunch lye as thickener

| Std | Run | A: Lye dosage wt% | B: Temperature (0C) | C: Time (hr) | Dropping point (0C) | BOD ppm |
| --- | --- | --- | --- | --- | --- | --- |
| 4 | 1 | 15 | 180 | 1 | 140.01 | 17.56 |
| 6 | 2 | 15 | 140 | 5 | 157.12 | 15.06 |
| 8 | 3 | 15 | 180 | 5 | 144.05 | 16.18 |
| 17 | 4 | 9 | 160 | 3 | 169.27 | 14.23 |
| 2 | 5 | 15 | 140 | 1 | 144.92 | 16.10 |
| 14 | 6 | 9 | 160 | 5 | 169.31 | 15.64 |
| 5 | 7 | 3 | 140 | 5 | 143.58 | 18.00 |
| 13 | 8 | 9 | 160 | 1 | 151.46 | 16.34 |
| 7 | 9 | 3 | 180 | 5 | 134.32 | 20.05 |
| 18 | 10 | 9 | 160 | 3 | 169.27 | 14.23 |
| 11 | 11 | 9 | 140 | 3 | 163.07 | 14.25 |
| 20 | 12 | 9 | 160 | 3 | 169.27 | 14.23 |
| 9 | 13 | 3 | 160 | 3 | 143.55 | 16.22 |
| 10 | 14 | 15 | 160 | 3 | 161.59 | 14.80 |
| 12 | 15 | 9 | 180 | 3 | 163.56 | 15.39 |
| 19 | 16 | 9 | 160 | 3 | 169.27 | 14.23 |
| 3 | 17 | 3 | 180 | 1 | 128.92 | 20.25 |
| 16 | 18 | 9 | 160 | 3 | 169.27 | 14.23 |
| 15 | 19 | 9 | 160 | 3 | 169.27 | 14.23 |
| 1 | 20 | 3 | 140 | 1 | 123.44 | 18.17 |

Table 8. RSM results for grease produced using NaOH as Thickener

| Std | Run | A: NaOH dosage wt% | B: Temperature (0C) | C: Time (hr) | Dropping point (0C) | BOD ppm |
| --- | --- | --- | --- | --- | --- | --- |
| 4 | 1 | 15 | 180 | 1 | 137.42 | 20.97 |
| 6 | 2 | 15 | 140 | 5 | 154.51 | 18.49 |
| 8 | 3 | 15 | 180 | 5 | 141.44 | 19.61 |
| 17 | 4 | 9 | 160 | 3 | 166.55 | 17.64 |
| 2 | 5 | 15 | 140 | 1 | 142.31 | 19.53 |
| 14 | 6 | 9 | 160 | 5 | 166.71 | 19.07 |
| 5 | 7 | 3 | 140 | 5 | 140.97 | 21.43 |
| 13 | 8 | 9 | 160 | 1 | 148.85 | 19.78 |
| 7 | 9 | 3 | 180 | 5 | 131.71 | 23.48 |
| 18 | 10 | 9 | 160 | 3 | 166.55 | 17.64 |
| 11 | 11 | 9 | 140 | 3 | 160.46 | 17.68 |
| 20 | 12 | 9 | 160 | 3 | 166.55 | 17.64 |
| 9 | 13 | 3 | 160 | 3 | 140.94 | 19.65 |
| 10 | 14 | 15 | 160 | 3 | 158.98 | 18.23 |
| 12 | 15 | 9 | 180 | 3 | 160.97 | 18.82 |
| 19 | 16 | 9 | 160 | 3 | 166.55 | 17.64 |
| 3 | 17 | 3 | 180 | 1 | 126.31 | 23.68 |
| 16 | 18 | 9 | 160 | 3 | 166.55 | 17.64 |
| 15 | 19 | 9 | 160 | 3 | 166.55 | 17.64 |
| 1 | 20 | 3 | 140 | 1 | 120.79 | 21.60 |

3.2.1 Analysis of variance (ANOVA) for the dropping point and BOD of the grease samples using palm bunch lye and NAOH.

To ensure a robust model fit, an analysis of variance (ANOVA) was performed to assess the individual model coefficients and test for lack of fit. The lack-of-fit test determines whether the model fails to adequately represent the data, excluding the random error factor (Tabrizi et al., 2011). The significance of the process variables was evaluated using the F-value and P-value (also referred to as "prob > F"). A higher F-value and a correspondingly lower P-value suggest a more significant model term (Tabrizi et al., 2011). Results from the second-order response surface model for the dropping point of the grease, as summarized in Tables 9 - 12, show F-values of 98.20, 98.45 and 76.39, 75.94 with P-values of <0.0001, indicating that the models are highly significant. The likelihood of such high F-values occurring due to random error is only 0.01%, supporting the reliability of the model. The Predicted R² values of 0.8952, 0.8950 and 0.8868, 0.8870 closely match the Adjusted R² values of 0.9787, 0.9788 and 0.9728, 0.9726 with differences of less than 0.1 and 0.2, respectively, indicating strong model accuracy. Furthermore, the Adeq Precision values, which assess the signal-to-noise ratio, were 29.6084, 29.6701 and 27.1588, 27.0537 well above the desired threshold of 4. This confirms that the models provide reliable predictions for the response variables (dropping points and BODs). Overall, the models effectively capture the relationship between the independent process variables and the response variable, ensuring high predictive performance. Model terms with P-values below 0.0500 are considered statistically significant.

Table 9. ANOVA for quadratic model: Dropping point of grease from cotton seed oil using palm bunch lye as thickener.

| Source | Sum of Squares | Df | Mean Square | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 4375.53 | 9 | 486.17 | 98.20 | < 0.0001 | significant |
| A-Lye dosage | 545.83 | 1 | 545.83 | 110.25 | < 0.0001 |  |
| B-Temperature | 45.24 | 1 | 45.24 | 9.14 | 0.0128 |  |
| C-Time | 355.57 | 1 | 355.57 | 71.82 | < 0.0001 |  |
| AB | 25.20 | 1 | 25.20 | 5.09 | 0.0477 |  |
| AC | 10.81 | 1 | 10.81 | 2.18 | 0.1703 |  |
| BC | 65.55 | 1 | 65.55 | 13.24 | 0.0045 |  |
| A² | 707.52 | 1 | 707.52 | 142.91 | < 0.0001 |  |
| B² | 77.10 | 1 | 77.10 | 15.57 | 0.0027 |  |
| C² | 186.04 | 1 | 186.04 | 37.58 | 0.0001 |  |
| Residual | 49.51 | 10 | 4.95 |  |  |  |
| Lack of Fit | 49.51 | 5 | 9.90 |  |  |  |
| Pure Error | 0.0000 | 5 | 0.0000 |  |  |  |
| Cor Total | 4425.03 | 19 |  |  |  |  |
| Std. Dev. | 2.23 |  | R² |  | 0.9888 |  |
| Mean | 154.23 |  | Adjusted R² |  | 0.9787 |  |
| C.V. % | 1.44 |  | Predicted R² |  | 0.8952 |  |
|  |  |  | Adeq Precision |  | 29.6084 |  |

Table 10. ANOVA for Quadratic model: Dropping point of the Produced Grease from cotton seed oil using NaOH as Thickener.

| Source | Sum of Squares | Df | Mean Square | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 4358.61 | 9 | 484.29 | 98.45 | < 0.0001 | significant |
| A-NaOH dosage | 546.71 | 1 | 546.71 | 111.14 | < 0.0001 |  |
| B-Temperature | 44.90 | 1 | 44.90 | 9.13 | 0.0129 |  |
| C-Time | 355.93 | 1 | 355.93 | 72.35 | < 0.0001 |  |
| AB | 25.28 | 1 | 25.28 | 5.14 | 0.0468 |  |
| AC | 10.95 | 1 | 10.95 | 2.23 | 0.1666 |  |
| BC | 65.90 | 1 | 65.90 | 13.40 | 0.0044 |  |
| A² | 705.44 | 1 | 705.44 | 143.40 | < 0.0001 |  |
| B² | 76.13 | 1 | 76.13 | 15.47 | 0.0028 |  |
| C² | 184.75 | 1 | 184.75 | 37.55 | 0.0001 |  |
| Residual | 49.19 | 10 | 4.92 |  |  |  |
| Lack of Fit | 49.19 | 5 | 9.84 |  |  |  |
| Pure Error | 0.0000 | 5 | 0.0000 |  |  |  |
| Cor Total | 4407.80 | 19 |  |  |  |  |
| Std. Dev. | 2.22 |  | R² |  | 0.9888 |  |
| Mean | 151.58 |  | Adjusted R² |  | 0.9788 |  |
| C.V. % | 1.46 |  | Predicted R² |  | 0.8950 |  |
|  |  |  | Adeq Precision |  | 29.6701 |  |

### Table 11. ANOVA for quadratic model: BOD of grease from cotton seed oil using palm bunch lye as thickener.

| Source | Sum of Squares | Df | Mean Square | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 69.47 | 9 | 7.72 | 76.39 | < 0.0001 | significant |
| A-Lye dosage | 16.87 | 1 | 16.87 | 167.00 | < 0.0001 |  |
| B-Temperature | 6.16 | 1 | 6.16 | 60.99 | < 0.0001 |  |
| C-Time | 1.22 | 1 | 1.22 | 12.05 | 0.0060 |  |
| AB | 0.3003 | 1 | 0.3003 | 2.97 | 0.1154 |  |
| AC | 0.5253 | 1 | 0.5253 | 5.20 | 0.0458 |  |
| BC | 0.0171 | 1 | 0.0171 | 0.1694 | 0.6894 |  |
| A² | 4.04 | 1 | 4.04 | 39.94 | < 0.0001 |  |
| B² | 0.7475 | 1 | 0.7475 | 7.40 | 0.0216 |  |
| C² | 7.87 | 1 | 7.87 | 77.86 | < 0.0001 |  |
| Residual | 1.01 | 10 | 0.1010 |  |  |  |
| Lack of Fit | 1.01 | 5 | 0.2021 |  |  |  |
| Pure Error | 0.0000 | 5 | 0.0000 |  |  |  |
| Cor Total | 70.48 | 19 |  |  |  |  |
| Std. Dev. | 0.3179 |  | R² |  | 0.9857 |  |
| Mean | 15.97 |  | Adjusted R² |  | 0.9728 |  |
| C.V. % | 1.99 |  | Predicted R² |  | 0.8868 |  |
|  |  |  | Adeq Precision |  | 27.1588 |  |

Table 12. ANOVA for Quadratic model: BOD of the Produced Grease from cotton seed oil using NaOH as Thickener

| Source | Sum of Squares | Df | Mean Square | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 69.82 | 9 | 7.76 | 75.94 | < 0.0001 | significant |
| A-NaOH dosage | 16.93 | 1 | 16.93 | 165.68 | < 0.0001 |  |
| B-Temperature | 6.13 | 1 | 6.13 | 60.01 | < 0.0001 |  |
| C-Time | 1.21 | 1 | 1.21 | 11.85 | 0.0063 |  |
| AB | 0.3081 | 1 | 0.3081 | 3.02 | 0.1131 |  |
| AC | 0.5151 | 1 | 0.5151 | 5.04 | 0.0486 |  |
| BC | 0.0153 | 1 | 0.0153 | 0.1499 | 0.7068 |  |
| A² | 4.05 | 1 | 4.05 | 39.68 | < 0.0001 |  |
| B² | 0.7553 | 1 | 0.7553 | 7.39 | 0.0216 |  |
| C² | 7.94 | 1 | 7.94 | 77.71 | < 0.0001 |  |
| Residual | 1.02 | 10 | 0.1022 |  |  |  |
| Lack of Fit | 1.02 | 5 | 0.2043 |  |  |  |
| Pure Error | 0.0000 | 5 | 0.0000 |  |  |  |
| Cor Total | 70.84 | 19 |  |  |  |  |
| Std. Dev. | 0.3196 |  | R² |  | 0.9856 |  |
| Mean | 19.39 |  | Adjusted R² |  | 0.9726 |  |
| C.V. % | 1.65 |  | Predicted R² |  | 0.8870 |  |
|  |  |  | Adeq Precision |  | 27.0537 |  |

3.2.2 Diagnostic reports of the RSM results for the dropping point and BOD of the grease

Figure 2  and 3 and figure 2 and 5 shows the Predicted verses Actual of the dropping point and BOD of the grease. The figures reveal the Axes: X-axis (Actual): The experimentally measured values dropping point and BOD. Y-axis (Predicted): The dropping point and BOD values predicted by the RSM model, based on the fitted polynomial equation. The dropping points and BOD values range were: 123.44,120.79 and 169.31, 166.71, 14. 23, 17.64 and 20.25, 23.68 respectively. The consistent alignment across the range shows that the model performs well for both low and high dropping point and BOD values. Most data points clustered around the line of best fit, indicating a good fit between the predicted and actual values (Dumancas, et al., 2016; Leung, et al., 2006; Fan, et al 2011; Eevera, et al., 2009). This suggests that the RSM model reliably predict the Dropping point and BOD of the grease. Table 13 and 14 shows the interactive effects of the process variables and validation of RSM data of the dropping point and BOD of the grease. This reveal how close the optimum (predicted) dropping point and BOD of the grease is to the experimental yield.  The determined percentage deviation is less than 5%. The RSM results were validated.

Figure 2. Parity plot of predicted versus actual dropping point for grease from palm bunch lye.

Figure 3. Parity plot of predicted versus actual for dropping point of grease from NaOH

Figure 4. Parity plot of predicted versus actual for BOD of the grease from palm bunch lye.

Figure 5. Parity plot of predicted versus actual of BOD for grease produced with NaOH

Table 13. Validation of the Dropping Point Results for the grease samples

| Samples | Lye or NaOH dosage (wt%) | Temperature (0C) | Time (hr) | Predicted dropping point (0C) | Experimental dropping point (0C) | Percentage deviation % |
| --- | --- | --- | --- | --- | --- | --- |
| Produced Grease using Lye as Thickener | 7.71 | 152.87 | 4.35 | 167.77 | 165.32 | 1.48 |
| Produced Grease using NaOH as Thickener | 9 | 160 | 3 | 166.32 | 169.85 | 2.08 |

Table 14. Validation of the BOD Results for the grease samples

| Samples |  | Lye or NaOH dosage (wt%) |  | Temperature (0C) |  | Time (hr) | Predicted dropping point (0C) |  | Experimental dropping point (0C) |  | Percentage deviation % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Produced Grease using Lye as Thickener | 7.71 |  | 152.87 |  | 4.35 |  |  | 14.94 | 15.45 | 3.30 |  |
| Produced Grease using NaOH as Thickener | 9 |  | 160 |  | 3 |  |  | 17.67 | 17.60 | 0.40 |  |

3.2.3 The 3-D plots for the dropping point of the grease using palm bunch lye and NaOH.

Figure 6 – 11 and figure 12 – 17  show the the three-dimensional plots of dropping point and BOD of the grease. The interactive effects of the process variables on the dropping point and BOD of the grease reveal parabolic graphs in each case. It then verified that there is a quadratic link between the response (Dropping point and BOD) and the factors taken into consideration in the formulation of the grease (Minodora, et al., 2010). The determined percentage is less than 5, the RSM result were validated.

Figure 6. Response surface plot of temperature and lye dosage for dropping point of grease using palm bunch lye.

Figure 7. Response surface plot of time and lye dosage for dropping point of grease using palm bunch lye.

Figure 8. Response surface plot of time and temperature for dropping point of grease using palm bunch lye.

Figure 9. Response surface plot of temperature and NaOH dosage for dropping point of grease from NaOH.

Figure 10. Response surface plot of time and NaOH dosage for dropping point of grease from NaOH.

Figure 11. Response surface plot of time and temperature for dropping point of grease from NaOH.

Figure 12. Response surface plot of temperature and lye dosage for BOD of grease using palm bunch lye.

Figure 13. Response surface plot of time and lye dosage for BOD of grease using palm bunch lye.

Figure 14. Response surface plot of time and temperature for BOD of grease using palm bunch lye.

Figure 15. Response surface plot of temperature and NaOH dosage for BOD of grease from NaOH.

Figure 16. Response surface plot of time and NaOH dosage for BOD of grease from NaOH.

Figure 17. Response surface plot of time and temperature for BOD of grease from NaOH.

4 CONCLUSION

This study evaluated and optimized the chemical synthesis of glycerin from the transesterification of cottonseed oil and bio-grease from palm bunch lye and sodium hydroxide as a thickening agent, with Moringa oleifera leaf extract as a rust-inhibiting additive. The glycerin yield values were predicted by the RSM model based on the fitted polynomial equation. An optimum glycerin yield of 48.51% was obtained at a methanol-to-oil ratio of 3:1, a catalyst dosage of 1.5 wt%, a temperature of 55°C, and a time of 60 minutes. The analysis of variance (ANOVA) for both glycerin yield and bio-grease properties confirms the reliability and robustness of the models used. For glycerin yield, the Predicted R² of 0.9556 is in close agreement with the Adjusted R² of 0.9831, with a difference of less than 0.2, indicating a strong model fit. For the dropping point and BOD of the grease, the Predicted R² values of 0.8952 and 0.8950 for dropping point and 0.8868 and 0.8870 for BOD closely match the Adjusted R² values of 0.9787 and 0.9788 for dropping point and 0.9728 and 0.9726 for BOD, with differences of less than 0.1 and 0.2, respectively, confirming that the model predictions are highly accurate. The consistent alignment across the range shows that the model performs well for both low and high dropping point and BOD values. Optimum dropping points of 167.77°C and 166.32°C were obtained for the grease sample, while 14.94 and 17.67 ppm were the corresponding optimum BOD values. The validation of RSM data for the dropping point and BOD of the grease reveals how close the optimum (predicted) glycerin yield, dropping point, and BOD of the grease are to the experimental yield. The determined percentage deviation is less than the critical value of 5%. The interactive effects of the process variables on the glycerin yield, dropping point, and BOD of the grease reveal parabolic graphs in each case. Therefore, the generated quadratic models adequately described the relationships between the responses (glycerin yield, dropping point, and BOD) of the grease sample and the considered factors. The grease produced using palm bunch lye performed better than grease from sodium hydroxide, showing superior biodegradability and model consistency (Kumar, et al., 2020).

| Acronym | Abbreviations |
| --- | --- |
| BOD | Biological oxygen demand |
| RSM | Response Surface Methodology |

REFERENCE

Abdullah, B.M., Salimon J., 2011. Optimization of process parameters for diesters biolubricant using D-optimal design. World Acad. Sci. Engr. Technol. 5(6), pp. 773-781.

Alamu, O. J., Waheed, M. A., Jekayinfa, S. O., 2007. Alkali-catalysed laboratory production and testing of biodiesel fuel from Nigeria palm kernel oil. Agricultural engineering international the CIGR Ejournal. EE07 009. 9 pp 1-11.

Akinpelu, Babayemi., Okechukwu Dominic Onukwuli., Eluno Emmanuel Eluno. 2021. Optimizing process parameters of palm oil bleaching on locally prepared animal bone based activated carbon using response surface methodology. Environmental Quality Management 10(2). http://dx.doi.org/10.1002/tqem.21729.

Awoyale, A.A., Odubiyi O.A.,  Eloka-Eboka A.C., 2011. Production and Testing of Biodegradable Grease from Black-Date (Canarium Schweinfurthii) Oil, Journal of Innovative Research in Engineering and Sciences, 2(4), 223-233.

Dumancas, G., Patel, V. Viswanath, L., Maples, R., & Subong., B. J., 2016. Castor Oil: Properties, Uses, and Optimization of Processing Parameters in Commercial Production. Lipid Insights, 1-12.

Eevera, T., Rajendran, K., Saradha, S., 2009. Biodiesel production process optimization and characterization to assess the suitability of the product for varied environmental conditions. Renewable energy, 34, 762 – 765.

Fan, X., Wang, X., & Chen, F., 2011. Biodiesel Production from Crude Cottonseed Oil: An Optimization Process Using Response Surface Methodology. The Open Fuels & Energy Science Journal, 4, 1-8.

Huei, R. O., Wan M.E.I., Choon P.G., Chi S.H., Md. Maksudur  R.K., Mohammad K.A.M., 2020. Preparation and Characterization of Grease using Used Cooking Oil and Used Engine Oil, J. Phys.: Conf. Ser, 1-6.

Jiabao. Pan., 2015. Polytechnic University. https://www.researchgate.net/publication/278741826 Effect of Heat Treatment on Lubricating properties of Lithium Lubricating grease. Article in RSC Advances. DOI: 10.1039/C5RA08917D.

Jurado-Alameda, E., Bravo-Rodríguez V., Bailón-Moreno R., Nuñez-Olea J., Altmajer V.D., 2003. Bath-substrate-flow method for evaluating the detersive and dispersant performance of hard-surface detergents. Ind. Eng. Chem. Res, pp. 4303-4310.

Ezeugo., Onukwuli1., Ikebudu., Ezechukwu3., Nwaeto., 2024. Optimization of Chrysophyllum albidum leaf extract as corrosion inhibitor for aluminium in 0.5 M H2SO4. World scientific news, 20(5).

Kumar, S.S., Jayaprakash R., Ramesp K.V., 2020. Experimental Study on Drop Point of Grease Samples for Various Lubricating Applications. IJERTCONV8IS16031.

Leung, D. Y. C., Guo, Y., 2006. Transesterification of neat and used frying oil: optimization for biodiesel production. Fuel processing technology, 87(10), 883 – 890.

Minodora, L., Luminiţa T., Marin M., Teodora S., 2010. Optimization of biodiesel production by transesterification of vegetable oils using lipases. Romanian Biotechnological Letters, 15 (5), 5618-5630.

Montgomery, D.C., 2001. Design and Analysis of Experiments (fifth ed.), John Willy and Sons, New York, USA.

Onukwuli, O. D. and Omotioma M., 2016. Optimization of the Inhibition Efficiency of Mango Extract as Corrosion Inhibitor of Mild Steel in 1.0M H2SO4 using Response Surface Methodology, Journal of Chemical Technology and Metallurgy, 51 (3), 302 – 314.

Omotioma .M., Okezue C.F., Obiora-Okafor I.A., 2021. Bamboo (Bambusoideae) Leaf on the Detoxification of Cassava Waste water for Potential Biogas Production, Journal of water Chemistry and Technology, 43 (1) 40-45 Springer.

Ozioko, F.U., 2012. Extraction and characterization of soybean oil based bio-lubricant AU J. Technol., 15(4), pp. 260-264.

Tabrizi, S. A. H., E. T. Nassaj., 2011. Modelling and optimization of densification of nanocrystalline Al2O3 powder prepared by a sol–gel method using response surface methodology. J. Sol-Gel. Sci. Technol. 57:212–220.