Original Research Article

A Sustainable Alternative: Violet Pigment from Streptomyces DP6 for Textile Applications

ABSTRACT

Introduction: The environmental impact of synthetic dyes have sparked interest in eco-friendly, biodegradable, non-toxic natural colorants. Microbial pigments hold considerable potential for applications in industries such as textile, food, and pharmaceuticals. In this study, a violet pigment producing Streptomyces violaceoruber strain DP6 was isolated, characterized and explored for its use in fabric dyeing. Material and Methods: Strain DP6 was isolated from a soil sample collected from Dalhousie, Himachal Pradesh, India. The strain producing a violet pigment was characterized using morphological, cultural, chemotaxonomic, and 16S rRNA sequencing methods. Various physical parameters were studied to obtain the maximum yield of the extracellular pigment. Dyeing potential of the pigment was evaluated on silk and wood fabrics. Further, pigment was purified and characterized. Results: Optimum pigment production was achieved when DP6 was cultivated for 10 days in ISP5 medium (International Streptomyces Project), at an initial pH of 5.0-5.5, with 2% inoculum, and incubated at 30oC under shaking conditions (160 rpm). The violet pigment was extracted using ethyl acetate and was found to be highly sensitive to changes in pH and sunlight. The dyeing ability of the violet pigment, produced under optimized conditions was evaluated on wool and silk fabrics. The color yield was observed to be better on wool as compared to silk. Additionally, mutagenicity tests confirmed the non-mutagenic nature of the pigment. Purification and preliminary characterization suggested that the pigment may possess an anthraquinone type structure with a methoxy group. Conclusions: The study results indicate that the violet pigment from Streptomyces DP6 hold potential to be exploited as a safe dye for use in the textile industry.

Keywords:  Sustainable dyeing, violet pigment, Streptomyces DP6

1. INTRODUCTION

The textile industry in India is the second largest sector after agriculture, generating huge employment opportunities for both types of skilled and unskilled labour. It offers employment to around forty five million people directly and around sixty million people indirectly in the country Colouring textile materials dates back to ancient times. Nowadays, the textile dyeing industry is facing challenges related to environmental issues. This industry is generating a substantial amount of contaminated water waste and also generating large amount of chemical waste (Kramar and Kostic, 2022; Islam et al., 2023). Dyed fabrics also contain toxic dye residues attached to the fabric and these chemicals can cause skin problems to consumers when they use dyed fabrics. Thus, use of these chemical or synthetic dyes in textile industry is posing significant threat to the environment and human health (Alihosseini et al., 2008; DeBritto et. al, 2020).

Pigment production from natural sources is gaining importance worldwide due to safety concerns triggered by use of artificial synthetic dyes. Natural dyes are safer and environment friendly because of their better biodegradability. Microorganisms are well known for producing secondary metabolities including pigments antibiotics and enzymes (Kanwar et al., 2024; Etta et al., 2025; Sharma et al., 2025). However, pigments from microorgansims are less explored as compared to plants and animals (Sen et al., 2019). Microoroganisms belonging to the Genus Serratia, Streptomyces, Pseudomonas, Chromobacterium and Janthinobacterium are known to produce a variety of both extracellular as well as intracellular pigment (Agarwal et al., 2023). Biopigments chemically attach to textile materials and form bonds with functional groups of fabric fibres. Additionally, these pigments also possess good antimicrobial, anticancerous and antioxidative properties (Stankovic et al., 2014; Mumtaz et al., 2019; Venil et al. 2021). Nowadays, researchers are isolating pigment producing microbes and exploring their dyeing potential (Kumar et al., 2018; Galasso et al., 2017; Mazotto et al., 2021). To make earth sustainable, the best option is to replace the harmful chemical dyes with natural dyes produced by microorganisms.

Among microorganisms, actinobacteria, especially Streptomyces spp. produce many intensely pigmented molecules that cover the visible light spectrum.  Ultramarine blue pigment actinorhodin and yellow pigment from Streptomyces coelicolor, red pigment rubrolone from Streptomyces echinoruber are examples of pigments reported from Streptomyces (Sarmiento-Tovar et al., 2022). The production of distinct cocktail of pigments by Streptomyces spp. has been employed as an important cultural characteristic in characterizing these microorganisms. Despite the multifarious potential of Streptomyces spp. in diverse fields, very few studies have been reported on the dyeing potential of pigments obtained from these organisms (Srinivasan et al., 2017; Hizbullah et al., 2018; Abou Elmaaty et al., 2020; Nuanjohn, et al., 2020). Therefore, the present study was carried out with the objective to assess the dyeing potential of violet pigment produced by an actinobacterium isolate (designated as DP6) on wool and silk fabrics. The isolate was identified as a strain of Streptomyces violaceoruber strain DP6.

2. MATERIALS AND METHODS

2.1 Isolation and characterization of DP6

The soil sample was collected from Dalhousie, Himachal Pradesh, India (32.53° N, 75.98° E) in sterile polyethylene bags, sealed tightly and stored in a refrigerator. Soil sample was given three different pretreatments and was serially diluted to 10-6 and then 0.1 ml aliquot from each dilution was spread on starchcasein medium containing (g/l): starch 10.0, casein 0.3, KNO3 2.0, NaCl 2.0, K2HPO4 2.0, MgSO4.7H2O 0.05, CaCO3 0.02, FeSO4.7H2O 0.01 and agar 18.0, which was supplemented with cycloheximide (50 µg/ml) and nystatin, (25 µg/ml) (Sharma et al., 2011; Kaur et al., 2013). The plates were incubated at 28°C for a period of 7 to 21 days. The resulting actinobacterial colonies were then subcultured and pure actinobacterial cultures were preserved using glycerol suspension (20% v/v) and stored at -80°C.

The DP6 isolate, producing violet pigment, was characterized using cultural and morphological methods from the International Streptomyces Project. For analysing morphological features, DP6 was grown on SCNA media and incubated at 28°C. After 4 days the culture morphological features were studied using a light microscope. Additionally, DP6 was grown on various ISP media for studying cultural characteristics such as soluble pigments, sporulation, aerial and substrate mycelia color etc. Various biochemical tests, including casein, lipid, and starch hydrolysis, nitrate reduction, gelatin liquefaction, and hydrogen sulfide production, were performed. Citrate utilization and urea hydrolysis were also assessed. Finally, diaminopimelic acid isomers in the cell wall and sugar composition in the whole-cell hydrolysate were analysed.

2.2 Phylogenetic analysis/DNA sequence analysis

The genomic DNA of DP6 was extracted and amplified using primers: f27 (5ˈ-AGAGTTTGATCATGGCTCAG-3ˈ) and r1492 (5ˈ-TACGGCTACCTTGTTACGACTT-3ˈ) and the amplified product was sequenced. The sequenced 16S DNA was compared against sequences from the EzTaxon database using BLAST (Chun et al., 2007). Almost complete DP6 sequence was aligned with downloaded sequences using the Clustal W program. Using the neighbor-joining method in MEGA 5 software, DP6 phylogenetic tree was constructed and bootstrap analysis was performed (Tamura et al., 2011). Finally, the 1401-bp sequence was deposited in GenBank with accession number JX683527.

2.3 Optimization of pigment production

For the development of inoculum, 50 ml of Glycerol Asparagine broth (ISP-5) having pH 7.0 was dispensed in 250 ml Erlenmeyer flasks and inoculated with 7 days old slant culture. For the pigment production, the same medium was inoculated with 48 hours old culture (1% v/v) and incubated at 28 °C on a rotary shaker (Scigenic biotech, Orbitek) at 180 rpm for 10 days. Various physical parameters viz. temperature, initial pH, fermentation time and agitation speed were studied to obtain the maximum yield of the extracellular pigment. Optimization of production was done by varying a single parameter at a time and keeping others constant. Pigment production was monitored by spectrophotometric measurements using a UV-Visible spectrophotometer (Shimadzu UV-1601, Japan).

2.4 Pigment sensitivity and extraction

The pH sensitivity of the pigment was checked by adjusting pH of culture supernatant from pH 2- 12 and absorbance spectra in the range of 300-700 nm was read by using UV-Visible spectrophotometer. The extent of photo-degradation under mercury light (ordinary tube light), UV-light and sun light was checked after 3 hours intervals until 9 hours.

For the extraction of pigment, 10 days old culture broth was centrifuged (10,000 rpm) for 20 minutes and pH of supernatant was adjusted to 3.0. The acidified supernatant was extracted with ethyl acetate in 2:1 ratio. Solvent containing pigment was dried on a rotary evaporator (Buchi, Switzerland) and re-dissolved in the water.

2.5 Mutagenicity testing

The study utilized strains TA98 (for frame-shift mutations) and TA100 (for base-pair substitution mutations), with 4-Nitro-o-phenylenediamine (NPD) and sodium azide serving as their respective diagnostic mutagens. The mutagenicity of the aqueous pigment extract was evaluated using Ames test. For the assay, 0.1 ml of the extract at varying concentrations (25, 50, 100, 250 μg/0.1 ml) and 100µl of bacterial suspension were mixed with 2 ml of top agar and spread on minimal agar plates (Rampal et al., 2017). These plates were incubated at 37°C for 48 hours. Negative controls (100µl bacterial culture + 100µl sterilized distilled water) and positive controls (20 μg/0.1 ml NPD for TA98 and 2.5 μg/0.1 ml sodium azide for TA100) were included. After 48 hours, the number of revertant his+ bacterial colonies was counted. The mutagenic potential of the pigment extract was determined by comparing the colony counts with those on control plates. The experiment was conducted in triplicate.

2.6 Fabric dyeing and color fastness testing

The fabrics were treated with 5g/L standard soap solution (SDC, Bradford) at 50°C for 30 minutes (Ndinchout et al., 2019). The material to liquor ratio was taken as 1:30. Fabrics was rinsed in cold water after washing and dried at room temperature. Pretreated samples were dyed for an hour at 100°C in an open bath beaker dyeing machine. Material to liquor ratio of the sample was 1:30. The pH of the dyeing bath was maintained upto 4.5 by using acetic acid. The dyed samples were thoroughly rinsed under running tap water. To improve washing fastness, soaping with standard soap solution (2 g/l) was done at 60ºC for 15 minutes. by using 1:30 material to liquor ratio.

Color fastness to washing was assessed by standard method of ISO CO6 C2S test (Bradford, 1990). Soap solution was made by adding 4 g/l ECE soap, 1 g/l Sodium perborate and 1 g/l sodium carbonate in 100 ml distilled water (pH 10) and heated at 60ºC  for 30 minutes. Dyed fabrics were subjected to light fastness standard test method ISO 105/ BO2 using a xenon arc lamp.

2.7 Reflectance values

Data color UV spectrophotometer (Perkin Elemer, USA) was used to measure the color of a sample using the CIELAB color space The reflectance of the soaped samples was measured on a and relative color strengths (K/S values) will be calculated using Kubelka Munk equation formula:

K/S= (1-R) 2 /2R

Where, R is the light reflectance of the dyed samples at max. K is the absorption coefficient and S is the scattering coefficient

2.8 Purification and Characterization

DP6 pigment was purified using Toyopearl resin HW-40 (Tosoh Bioscience, Germany) and reverse phase-HPLC (1260 Infinity Agilent Technologies, United States). The mobile phase consisted of HPLC grade water and acetonitrile, with 0.1% and 0.12% trifluoroacetic acid as mobile phases A and B, respectively (Sharma et al., 2024). The injected sample peaks were monitored (UV detector set at 220 nm) and collected for further analysis. The colored peak (RT 19.8 minutes) was collected, concentrated, redissolved and injected it onto HPLC to check its purity. 1H NMR was performed to study the structure of the pigment. For NMR, AVANCE III Bruker spectrometer (Bruker, Germany) at 25 °C on 500 MHz was used, and the sample was dissolved in chloroform-d (99.8 atom% D, containing 0.1% (v/v) tetramethylsilane TMS.

3. RESULTS AND DISCUSSION

3.1 Identification of strain

The cultural characteristics of isolate DP6 were investigated on various ISP media. DP6 exhibited robust growth on all ISP media. However, no melanin pigment production was observed on Peptone Iron Agar (ISP-6) or Tyrosine Agar (ISP-7) media (Table 1). Notably, the maximum growth and violet pigment production occurred on Glycerol asparagine medium (ISP-5) (Fig. 1a). Microscopic examination revealed short, slightly spiral chains of spores with approximately 20-30 spores on the aerial mycelium (Fig. 1b).

Chemotaxonomic analysis revealed presence of LL-diaminopimelic acid as the characteristic diamino acid in the cell wall. No characteristic sugar was identified in the whole-cell hydrolysate. DP6 also produced various extracellular enzymes, including protease, amylase, lipase, urease and gelatinase. Nevertheless, it did not respond to cellulase. DP6 showed positive results citrate utilization and H2S production (Table 2).

Table 1 Cultural characteristics of DP6 on different ISP media

| Characteristic | ISP-1 | ISP-2 | ISP-3 | ISP-4 | ISP-5 | ISP-6 | ISP-7 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Growth | Good | Good | Good | Good | Good | Good | Good |
| Color of aerial mycelium | White | Grey | Grey | Grey | Grey | Grey | Grey |
| Color of substrate mycelium | Blue | Violet | Violet | Violet | Violet | Light brown | Orange |
| Soluble pigment | Blue | None | None | Violet | Violet | None | None |
| Sporulation | White | Grey | Grey | Grey | Pink white | Grey | Grey |

Table 2 Morphological, physiological and biochemical characteristics of Streptomyces DP6

| Characteristic | Result |
| --- | --- |
| Spore mass | Pinkish white |
| Spore chain Spores shape | Short/ slightly spiral Round |
| Substrate mycelium | Violet |
| Aerial mycelium | Violet |
| Pigment | Violet |
| Sugar pattern | No sugar |
| Diaminopimelic acid | LL-DAP |
| Production of melanin pigment on : Tyrosine agar medium Peptone yeast extract agar medium | - - |
| Production of hydrolytic enzymes: Amylase Protease Cellulase Lipase | + + - + |
| Gelatinase | + |
| Urease Pectinase | + - |
| H2S production | + |
| Citrate utilization Indole Growth Temperature | - - 25oC (20 to 35 oC) |

Fig. 1. Phylogenetic tree obtained by Neighbor joining analysis of 16S rRNA gene sequences showing the relationship between DP6 and species belonging to the genus Streptomyces. (a) Inset showing violet pigment production by Streptomyces DP6 (b) Aerial mycelium of Streptomyces DP6 showing spiral spore chains (at 100X)

Based on morphological, cultural, and chemotaxonomic studies, strain DP6 was classified within the genus Streptomyces. This classification was further supported by 16S rRNA sequencing. DP6 sequence (1401 bp) exhibits 99-100% similarity with other Streptomyces spp. available at EzTaxon database. Notably, DP6 was most closely related (100%) to Streptomyces violaceoruber NBRC 12826 T (AB184174). A phylogenetic tree constructed using the neighbor-joining method to confirm its close relationship with other species (Fig. 1c). Further comparison between DP6 and S. violaceoruber revealed similarities in most cultural characteristics. However, S. violaceoruber lacked violet pigment production on ISP-5 medium. Additionally, DP6 exhibited differences in physiological traits, including H2S production and urea hydrolysis, whereas S. violaceoruber did not produce H2S or hydrolyze urea. Based on these findings, actinobacterium DP6 was identified as a strain of S. violaceoruber.

3.2 Optimization of pigment production

The production of violet pigment started on third day of incubation and continued to increase, and reached to its highest level at tenth day. The UV-VIS analysis of the samples obtained after every 24 h showed two constant peaks, one with λmax 404 nm and another with λmax 535 nm. To determine the effect of initial pH of the medium on production, fermentation was carried out over a range of pH 4.0- 8.0. The maximum pigment yield and growth (2.92 g/l) was achieved at pH 5.0 and pH 6.0, respectively (Fig. 2a). The quality of the pigment varied with change of pH.  Pink to violet colored pigment with   λmax 404 and λmax 535 was produced at acidic pH (4.0-6.0) but higher pH supported the production of blue pigment with λmax 535 nm. In accordance to our results, Chatterjee et al. (2009) also reported the influence of initial pH of the fermentation medium on quality of the pigment produced by Monascus purpureus. They obtained more yellow pigment (λmax 400 nm) at acidic pH (2.0- 4.0), whereas at higher pH (6.0- 8.0) the red pigment (λmax 500 nm) was dominating. The orange fraction (λmax 480 nm) maintained steadily irrespective of pH condition.

Temperature plays a vital role in cell metabolism, thus influencing pigment production (Chatterjee et al., 2009). The maximum pigment and biomass production (1.3 g/l) from Streptomyces DP6 was recorded at 30ºC and rate of production was reduced as the temperature increased. No pigment was produced at 40 ºC (Fig. 2b). Variation in temperature did not affect the color of the pigment. To check the influence of agitation on growth and pigment production, Streptomyces DP6 was grown at various agitation rates. The pigment yield and growth varied at different agitation rates (Fig. 3). The highest growth (1.3 g/l) and pigment production was obtained at 160 rpm and reduced thereafter with further increase in agitation. The highest levels of violacein (violet pigment) from Pseudoalteromonas luteoviolacea under static conditions and decrease in yield with the increase of agitation speed (Yang et al., 2007).

Fig. 2. Effect of pigment production and mycelial growth (a) Initial pH of medium (b) Incubation temperature

Fig. 3. Effect of agitation on the pigment production and mycelial growth

3.3 pH sensitivity and photochemical degradation of the pigment

The pigment isolated from Streptomyces DP6 was found to be very sensitive to pH change (Fig. S2). The color of the pigment changed according to the variation in the pH of the supernatant along with change in color as follows; at pH 2-6, pink (λmax 532- 235 nm); pH 6, light violet (λmax 535 nm); pH 7, violet (λmax 575 nm); pH 8, pale blue (λmax 579 nm); pH 10, blue (λmax 591 nm) and pH 12, blue (λmax 610 nm). Similar observation was reported for the anthocyanin pigments, widely used as food colorant, in that they are highly colored at pH values from 4-6 but almost colorless at high pH values (Carlsen and Stapelfeldt,1997) Similarly, the color of the pigment from Paecilomyces sinclairii was found to be dependent on pH of the solution; red at pH 3- 4 ( λmax 500, 507 nm); violet at pH 5-7 ( λmax 522, 526, 529 nm); pale violet at pH 8- 9 (λmax 536, 537 nm) and pale pink at pH 10- 12 (λmax 540, 541, 542 nm) (Cho et al., 2002).This might be possible because of the presence of different colored components present in the extract, concentrations of which vary at different pH values thus resulting in the corresponding shifts in absorption maxima. Due to this property of exhibiting different colors at different pH, the pigment from DP6 can be used as a pH indicator.

The photochemical degradation of pigment under mercury lamp, UV-light and sun light was checked spectrophotometrically after three hours intervals until 9 hours. It was observed that after three hours of irradiation, chromophore degradation under sun light began with corresponding shift of λmax from initial 525 nm to 502 nm, whereas in case of mercury lamp and UV-light no significant change took place. On further exposure, pigment showed even higher degradation under sun-light and negligible change in case of mercury lamp and UV-light. Thus, it is concluded that pigment is highly sensitive to sun-light and comparatively stable when exposed to mercury lamp and UV-light. After 9 hours, the percent degradation under mercury lamp, UV-light and sun light were 12.1%, 8.4% and 22.0%, respectively. It would, therefore be suggested to protect the products colored with the pigment from intense sun light as much as possible or the pigment should be complexed with some light protective agent or mordant before use. Photochemical degradation of dye gardenia blue, phycocyanin and indigo dye has also been reported Dellamatrice, et al., 2017; Ali et al., 2011).

3.4 Dyeing potential analysis

Dyeing ability of the pigment extract was assayed by directly applying it on wool and silk fabrics. The pigment showed dyeing ability for both fabrics. Color yield was found to be better on wool as compared to silk because of amphoteric nature of wool. Similarly, Yosuf et al., also reported fabric depended varying dyeing capability of pigment from Serratia marcescens.  Red and yellow pigment obtained from fungal strains Monascus purpureus and Penicillium purpurogenum, respectively, also showed dyeing potential for cotton and leather products when used in combination with ferrous sulphate as mordant (Velmurugan et al., 2009). Dyeing and printing efficiency of the brown pigment produced by a Streptomyces strain was also reported (Periyasamy et al., 2024). In another study, Abou Elmaaty et al. (2020) also evaluated the dyeing potential of orange pigment obtained from Streptomyces thingirensis on wool.

3.5 Washing and light fastness testing of the dyed fabrics

The results of fastness studies indicate very good washing fastness for both the dyed samples  while light fastness  was moderate to good (Table 3). The color fastness, including washing and light, of the dyed wool and silk samples was performed according to grey scale and presented in Table 4. The results indicted very good washing fastness for both the dyed samples with values ranging from 4-5 on grey scale. However, the results of light fastness for the samples indicate moderate to good values according to grey scale. Similar results were observed when wool fabrics was dyed with pigment from Streptomyces thingirensis Abou Elmaaty et al. (2020).

Table 3: Dyeing and fastness gradings of dyed fabrics

*SCA: Secondary Cellulose Acetate; BUC: Bleached Unmercerized cotton; N: Nylon; P: Polyester; A: Acrylic; WW: Worsted Wool (Compared with standard of Grey scale ratings in fabric dyeing)

** Grade 5: Excellent; 4: Better; 3: Good; 2: Ok; 1: poor

| Sample | Dyed Fabrics | Color Fastness | Washing Fastness |  |  |  |  |  | Light Fastness |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | SCA | BUC | N | P | A | WW |  |
| Wool |  | 2-3 | 4-5 | 4-5 | 5 | 5 | 4-5 | 4 | 3-4 |
| Silk |  | 3 | 4-5 | 5 | 5 | 5 | 5 | 4 | 3 |

3.6 Spectrophotometric K/S Analysis

The color properties of dyed wool and silk samples were quantified using the CIELAB system (Table 4). The color coordinates indicated the dyed wool was more deeply dyed than the silk at the given temperature, as indicated by greater chroma (C*). Dyed substrates were evaluated for K/S values by using spectrophotometer which showed higher K/S value for dyed wool as compared to silk (Fig. 4).

Table 4: Colorimetric data of dyed fabrics

| D65 10 Deg | L* | a* | b* | C* | H | X | Y | Z | x | Y |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Wool | 66.68 | 5.00 | 13.93 | 14.80 | 70.26 | 35.79 | 36.21 | 28.54 | 0.3560 | 0.3601 |
| Silk | 79.57 | 2.25 | 7.42 | 7.75 | 73.14 | 53.90 | 55.93 | 52.27 | 0.3325 | 0.3450 |

Colorimetric data represented using CIELAB color system, where

L* indicates - White/black,   a* - Red/Green,   b* - Blue/ yellow,     C* - Chroma   H - Hue, X, Y, Z, x, y: coordinates

Fig. 4. K/S values of dyed fabrics

3.7 Toxicity testing of the pigment

Mutagenicity testing done by Ames test showed  non mutagenic nature of the pigment at all the studied concentrations (25, 50, 100 and 200 µg/ 0.1ml) used in the experiment, as the number of revertant colonies in plates with pigment concentrations were found to be similar to that of spontaneous revertant colonies for TA98 as well as TA100 (Table 5). On contrary, most of the textile dyes are highly toxic and potentially carcinogenic and pose potential threat to the environmental as well as to human health (Periyasamy et al., 2024). Therefore, the non-mutagenic nature of the pigment point towards its promising potential to be used as a safe pigment/dye in the textile industries.

Table 5: Mutagenic Testing of DP6 Pigment

| Treatment | Dose (µg) | No. of colonies |  |
| --- | --- | --- | --- |
|  |  | TA98 | TA100 |
| Spontaneousa |  | 26.0 ± 1.0 | 187.33± 2.0 |
| Positive control (NPD)b | 20 | 950.33 ± 2.5 |  |
| Positive controlb (Sodium azide) | 2.5 |  | 1115.33± 4.0 |
| DP6 Pigment Extractc | 25 50 100 250 | 22.33 ± 2.5 25 ± 1.6 24.0 ± 2.5 24.63 ± 1.5 | 187.66 ± 4.0 185.0 ± 4.5 186.66 ± 2.5 190.33 ± 7.6 |

Values are mean ± S.D

aMean number of spontaneous revertants as determined in assays without pigment extract and   standard mutagen

bMean number of revertants induced by reference mutagens: NPD (20 μg) and Sodium azide

cMean number of revertants induced by DP6 pigment extract at different concentrations

3.8 Purification and structure of pigment

The pigment culture filtrate was recovered using XAD-4 (5% v/v) resin, purified by size exclusion chromatography (Toyopearl resin HW-40) and reverse phase-HPLC. The HPLC purified peptide showed retention peak at 17.3 minutes (Fig. 4). . 1H NMR showed the doublets at δ 7.14 and 7.38 respectively, and some multiplets of remaining aromatic protons are showed at δ 1.0-11.9 (Fig. 5). Proton NMR indicate presence of the singlet of methoxy group at δ 4.04. It is suggested that the DP6 pigment may be like an anthraquinone type structure with methoxy group. A structurally related compound to DP6, exhibiting antimicrobial and antiproliferative property, was previously isolated and reported from Streptomyces olivochromogenes (Balachandran et al., 2016).

Fig. 4. RP-HPLC profile of the purified pigment

Fig. 5.  1H NMR of the purified pigment

4. Conclusion

Microbial pigments are sustainable alternative to chemical dyes and could be used in the textile industry. Considering this fact, violet pigment produced by Streptomyces DP6 was explored for fabric dyeing.  The results revealed, Streptomyces DP6 pigment potential in dyeing wool and silk fabrics. The pigment was found to be safe and eco-friendly.  Most previous studies have focussed on the antimicrobial activity of the pigments. However, this research highlights the dyeing potential of Streptomyces DP6 pigment. Furthermore, the pigment's sensitivity to pH changes may allow it to function as a pH indicator, thereby expanding its potential applications.

Disclaimer (Artificial intelligence)

Author(s) hereby declare that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc.) and text-to-image generators have been used during the writing or editing of this manuscript.

REFERENCES

- Kramar, A., and Kostic, M. M. (2022). Bacterial Secondary Metabolites as Biopigments for Textile Dyeing. Textiles, 2(2), 252-264. https://doi.org/10.3390/textiles2020013

- Islam, T., Repon, M., Islam, T, Sarwar, Z. and Rahman, M. M. (2023). Impact of textile dyes on health and ecosystem: a review of structure, causes, and potential solutions. Environmental Science and Pollution Research International, 30, 9207-9242. https://doi:10.1007/s11356-022-24398-3

- Alihosseini, F., Ju, K. S., Lango, J., Hammock, B. D. and Sun, G.  (2008) Antibacterial colorants: characterization of prodiginines and their applications on textile materials. Biotechnology Progress, 24,742-747. https://doi: 10.1021/bp070481r

- DeBritto, S., Gajbar, T. D., Satapute, P., Sundaram, L., Lakshmikantha, R. Y., Jogaiah, S. and Ito, S. I. (2020). Isolation and characterization of nutrient dependent pyocyanin from Pseudomonas aeruginosa and its dye and agrochemical properties. Scientific Reports, 10(1), 1542. https://doi: 10.1038/s41598-020-58335-6

- Etta, K. K., Chetapalli, C., Muvva, V. and Kumbha, N. (2025).Taxonomic profile and antimicrobial potential of Brachybacterium conglomeratumVLCH–15 Isolated from Mangroves of Machilipatnam, Andhra Pradesh, India. Journal of Advances in Microbiology, 25 (2), 22-33. https://doi.org/10.9734/jamb/2025/v25i2898

- Sharma, D., Kanwar, K., and Manhas R. K. (2025). Genomic analysis of Streptomyces amritsarensis MTCC 11845 and characterization of novel lanthipeptide 2A. Indian Journal of Experimental Biology,  63, 229-238 https://doi.org/10.56042/ijeb.v63i03.13585

- Kanwar, K., Sharma, D., Singh, H., Pal, M., Bandhu, R. and Azmi, W. (2024) In vitro effects of alginate lyase SG4+ produced by Paenibacillus lautus alone and combined with antibiotics on biofilm formation by mucoid Pseudomonas aeruginosa. Brazilian Journal of  Microbiology, 5(2), 1189-1203. https://doi: 10.1007/s42770-024-01334-w

- Sen, T., Barrow, C. J. and Deshmukh, S. K. (2019) Microbial pigments in the food industry-challenges and the way forward. Frontier in Nutrition, 6, 7. https://doi:10.3389/fnut.2019.00007

- Agarwal, H., Bajpai, S., Mishra, A., Kohli, I., Varma, A., Fouillaud, M., Dufossé, L., and Joshi, N. C. (2023). Bacterial Pigments and Their Multifaceted Roles in Contemporary Biotechnology and Pharmacological Applications. Microorganisms, 11(3), 614. https://doi.org/10.3390/microorganisms11030614

- Venil, C. K., Dufossé, L., Velmurugan, P., Malathi, M., and Lakshmanaperumalsamy, P. (2021). Extraction and Application of Pigment from Serratia marcescens SB08, an Insect Enteric Gut Bacterium, for Textile Dyeing. Textiles, 1(1), 21-36. https://doi.org/10.3390/textiles1010003

- Stankovic, N., Senerovic, L., Ilic-Tomic, T., Vasiljevic, B. and Nikodinovic-Runic, J. (2014) Properties and applications of undecylprodigiosin and other bacterial prodigiosins. Applied Microbiology and Biotechnology, 98(9), 3841-358. https://doi: 10.1007/s00253-014-5590-1

- Mumtaz, R., Bashir, S., Numan, M., Shinwari, Z. K. and Ali, M. (2019). Pigments from soil bacteria and their therapeutic properties: a mini review. Current Microbiology, 76(6):783-790. https://doi: 10.1007/s00284-018-1557-2

- Kumar, A., Vishwakarma, H. S., Singh, J., Dwivedi, S. and  Kumar, M. (2015). Microbial pigments: production and their applications in various industries. International Journal of Pharmaceutical Chemical and Biological Sciences, 5,  203–212.

- Galasso, C., Corinaldesi, C. and Sansone, C. (2017). Carotenoids from marine organisms: biological functions and industrial applications. Antioxidants (Basel), 6(4), 96. https://doi: 10.3390/antiox6040096

- Mazotto, A. M., De Ramos Silva, J., De Brito, L. A. A., Rocha ,N. U. and De Souza Soares, A. (2021). How can microbiology help to improve sustainability in the fashion industry? Environmental Technology and Innovation, 23, 101760. https://doi: 10.1016/j.eti.2021.101760

- Sarmiento-Tovar, A. A., Silva, L., Sánchez-Suárez, J., and Diaz, L. (2022). Streptomyces-Derived Bioactive Pigments: Ecofriendly Source of Bioactive Compounds. Coatings, 12(12), 1858. https://doi.org/10.3390/coatings12121858

- Hizbullah, U. M., Farouq, A. A. A., Baki, S., Dabai, M. U., Nafi’u, A.,  Nata’ala, M. K. and Mustapha, G. (2018). “Studies on Bio-Color Production by Pseudomonas Aeruginosa isolated from Soil”. Journal of Advances in Microbiology 12 (1):1-12. https://doi.org/10.9734/JAMB/2018/43068

- Srinivasan, M., Keziah, S. M, Hemalatha, M. and Devi, C. S. (2017). Pigment from Streptomyces bellus MSA1 isolated from marine sediments. IOP Conference Series: Material Science and Engineering, 263, https://022049.doi:10.1088/1757-899X/263/2/022049

- Abou Elmaaty, T., Kasem, A., Elsalamony, M. and Gamal, H. A. (2020) Green Approach for One Step Dyeing and Finishing of Wool Fabric with Natural Pigment Extracted from Streptomyces thinghirensis. Egyptian Journal of Chemistry, 63(6), 1999-2008. https://doi: 10.21608/ejchem

- Nuanjohn, T., Suphrom, N., Nakaew, N., Pathom-Aree, W., Pensupa, N., Siangsuepchart, A., Dell, B., and Jumpathong, J. (2023). Actinomycins from Soil-Inhabiting Streptomyces as Sources of Antibacterial Pigments for Silk Dyeing. Molecules, 28(16), 5949. https://doi.org/10.3390/molecules28165949

- Sharma, D., Kaur, T., Chadha, B. S. and Manhas, R. K. (2011). Antimicrobial activity of actinomycetes against multidrug resistant Staphylococcus aureus, E. coli and various other pathogens. Tropical Journal of Pharmaceutical Research, 10, 801-808. https://doi:10.4314/tjpr.v10i6.14

- Kaur, T., Sharma, D., Kaur, A. and Manhas R. K. (2013) Antagonistic and plant growth promoting activities of endophytic and soil actinomycetes. Archives of Phytopathology and Plant Protection, 46, 1756-1768. https://doi:10.1080/03235408.2013.777169

- Sharma, D., Mayilraj, S., Manhas, R. K. (2014). Streptomyces amritsarensis sp. nov., exhibiting broad-spectrum antimicrobial activity. Antonie Van Leeuwenhoek 105(5):943-9. https://doi:10.1007/s10482-014-0151-2.

- Chun, J., Lee, J. H., Jung Y, Kim, M., Kim, S. and Lim, Y.W. (2007). EzTaxon: a web-based tool for the identification of prokaryotes based on 16S ribosomal RNA gene sequences. International Journal of Systematic and Evolutionary Microbiology, 57, 2259-2261. https://doi: 10.1099/ijs.0.64915-0.

- Tamura, K., Peterson, D., Peterson, N., Stecher, G., Nei, M. and Kumar, S. (2011) MEGA5: molecular evolutionary genetics analysis using maximum likelihood, evolutionary distance, and maximum parsimony methods. Molecular Biology and Evolution, 28, 2731-2739. https://doi:10.1093/molbev/msr121

- Rampal, G., Singh, T. T., Arora, R., Vig, A. P. and Arora, S. (2017). Synergistic antimutagenic effect of isothiocyanates against varied mutagens, Food and Chemical Toxicology, 109, 879-887. https://doi: 10.1016/j.fct.2017.05.017

- Ndinchout, A. S., Chattopadhyay, D. P., Paul, M. F., Ascension, N. M., Kaur, V. and Kaur, S. (2019). Studies on dyeing and bacterial resistance of Dacryodes macrophylla extract on woollen fabric. Journal of Applied and Natural Science, 11(1), 205-210. https://doi.org/10.31018/jans.v11i1.1993

- Sharma, D. (2024) Novel natural and synthetic anticandidal therapeutic peptides to combat drug-resistant infections. Medical Science Forum, 24, 12. https://doi:10.3390/ECA2023-16385.

- Chatterjee, S., Maity, S., Chattopadhyay, P., Sarkar, A., Laskar, S., Sen, S. K. (2009) Characterization of red pigment from Monascus in submerged cultured pigment from Monascus purpureus. Journal of Applied Sciences Research, 40, 132-138.

- Yang, L. H., Xiong, H., Lee, O. O., Qi, S. H. and Qian, P. Y. (2007). Effect of agitation on violacein production in Pseudoalteromonas luteoviolacea isolated from a marine sponge. Letters in Applied Microbiology, 44(6), 625-30. https://doi:10.1111/j.1472-765X.2007.02125.x

- Francis, F. J. (1989). Food colorants: anthocyanins. Critical Reviews in Food Science and Nutrition, 28(4), 273-314. https://doi: 10.1080/10408398909527503.

- Carlsen, C. and Stapelfeldt, H. (1997). Light sensitivity of elderberry extract quantum yields for photodegradation in aqueous solution. Food Chemistry, 60:383-387. https://doi:10.1016/j.foodres.2018.02.035

- Cho, Y. J., Park, J. P., Hwang, H. J., Kim, S. W., Choi, J. W. and Yun, J. W. (2002). Production of red pigment by submerged culture of Paecilomyces sinclairii. Letters in Applied Microbiology. 35, 195-202. https://doi:10.1046/j.1472-765x.2002.01168.x.

- Dellamatrice, P. M., Silva-Stenico, M.E, Moraes, L. A., Fiore, M. F. and Monteiro, R. T. (2017). Degradation of textile dyes by cyanobacteria. Brazilian Journal of Microbiology, 48(1), 25-31. https://doi:10.1016/j.bjm.2016.09.012

- Ali, M. A., Keera, A. A., Helmy, M. S., Abd El-Nasser, H. N., Ahmed, K. A. and El-Hennawi H. M. (2011) Selection of pigment (melanin) production in Streptomyces and their application in printing and dyeing of wool fabrics. Research Journal of Chemical Sciences, 1, 22-28.

- Velmurugan, P., Chae, J., Lakshmanperumalsamy, P., Yun, B., Lee, K. and Oh, B. (2009). Assessment of the dyeing properties of pigments from five fungi and anti-bacterial activity of dyed cotton fabric and leather. Color Technology, 125, 334-341. https://doi:10.1111/j.1478-4408.2009.00215.x

- Sharma, B., Dangi, A. K. and Shukla, P. (2018) Contemporary enzyme based technologies for bioremediation: A review. Journal of Environmental Management, 15, 210:10-22. https://doi: 10.1016/j.jenvman.2017.12.075-22.

- Periyasamy, A. P.  (2024). Recent advances in the remediation of textile-dye-containing wastewater: prioritizing human health and sustainable wastewater treatment. Sustainability, 16(2), 495. https://doi:10.3390/su16020495

- Balachandran, C., Duraipandiyan, V., Arun, Y., Sangeetha, B., Emi, N., Al-Dhabi, N. A., Ignacimuthu, S., Inaguma, Y., Okamoto, A. and Perumal, P. T. (2016). Isolation and characterization of 2-hydroxy-9,10-anthraquinone from Streptomyces olivochromogenes (ERINLG-261) with antimicrobial and antiproliferative properties. Revista Brasileira de Farmacognosia, 26(3), 285-295. https://doi.org/10.1016/j.bjp.2015.12.003.