Original Research Article

Assessing the Resilience Of Palm-Kernel – Based Concrete To Sodium Chloride And Sulphuric Acid Attack

# Abstract

This study seeks to address this gap and contribute to knowledge by expanding the application of this sustainable concrete type to include its durability and resilience in NaCl and H2SO4 containing conditions. The resilience of palm kernel-based concrete to environments containing sodium chloride (NaCl) and sulphuric acid (H2SO4) solutions is evaluated in this study. These solutions when in contact with concrete may compromise the performance of the concrete. Therefore, in the bid to include palm kernel shell-based concrete as a sustainable alternative material to traditional concrete material, it is essential to assess its durability in different exposure conditions. Palm kernel shell aggregates replaced 0 to 20 % of natural coarse aggregates and the fresh and hardened properties of the resulting concrete were evaluated. Additionally, the different concrete specimens produced were exposed to 5% NaCl and 5% H2SO4 solutions for a period of 7, 14 and 28 days. The change in mass and compressive strength after these periods were evaluated. Experimental results indicated that when exposed to the solutions, the PKS-based concrete experienced mass loss, with sulfuric acid causing greater deterioration (6.13% to 26.65%) mass loss) than sodium chloride (0.22% to 0.54%). Compressive strength reductions followed a similar trend, with the H₂SO₄-exposed samples showing more significant strength degradation.

Keywords: Palm kernel shell aggregates, concrete, compressive strength, flexural tensile strength, Sodium chloride attack, sulphuric acid attack.

# Introduction

The development of sustainable building materials has been aided in part by including industrial debris in concrete-making techniques in recent times (Kabbo et al., 2025). The increasing demand for durable structures emphasizes the importance of using materials resilient to corrosive environments. Concrete is particularly vulnerable to chemical attacks, notably from acidic substances prevalent in industrial areas and alkaline chemicals in wastewater treatment facilities (Ziamiavaghi & Toufigh, 2024). Research studies in concrete technology advancement seek to investigate the use of alternative sustainable materials for the production of concrete while evaluating its suitability for diverse concrete applications. Many research studies have considered the use of varying sustainable materials which includes Palm kernel shells (PKS) (Fapohunda et al., 2021; Hamada et al., 2018; Okina et al., 2024). PKS have been used to particularly replace natural coarse aggregates in concrete production (Chinnu et al., 2021; Zawawi et al., 2020). Interestingly, coarse aggregates account for about 70 – 80% of the total volume of concrete (Alqarni et al., 2022; Kim et al., 2019). In the bid to safeguard the environment from the depletion of natural resources, their replacement with PKS as coarse aggregates in concrete production serves as a sustainable solution. Additionally, the use of PKS which is a waste material resolves the challenges related to the disposal of waste materials (Hamada et al., 2018; Okina et al., 2024). These challenges include finding a suitable location for waste storage and managing and reducing the total volume of waste generated (Kalisha & Munthali, 2024; Kumar et al., 2017).  Concrete exhibits higher sustainability in terms of energy consumption and carbon emissions per unit volume than alternative construction materials, such as steel. Nevertheless, the extensive use of concrete in comparison with other construction materials has negated its sustainable advantage. Environmentally friendly concrete provides exceptional fresh and hardened properties compared with traditional concretes, thereby reducing maintenance expenses and construction timelines and providing an extended lifespan (Magbool et al., 2024).

Many research studies on the use of PKS in concrete production have explored its use for varying components of concrete as fine and coarse aggregates, supplementary cementitious material when ground into fine powder and many other uses (Azunna, 2019; Bediako et al., 2016; Boateng et al., 2023; Gibigaye et al., 2017; Olutoge et al., 2020). For these research studies, the fresh properties, which include workability and setting time, have been explored. In terms of the physical and hardened property evaluation, there have been studies on the density, porosity, water absorption, compressive strength, modulus of elasticity, split tensile strength, and modulus of rupture of palm kernel-based concrete (Alqarni et al., 2022; Kim et al., 2019; Okina et al., 2024).  Most research studies have shown that the density of PKS-based concrete is classified as lightweight with values between 1450 kg/m3 to 2042 kg/m3 depending on the replacement level of the PKS (Alsalami et al., 2018; Armah et al., 2019; Ogundipe et al., 2021). Alsalami, Harith and Dhahir (2018), reported that PKS, PKS ash used to produce concrete resulted in compressive strengths which were about 28 – 40 % lower than traditional concrete. For replacement levels which result in the optimum mechanical strength, past researchers have indicated that replacement levels beyond 20% is accompanied by reduced mechanical strength (Fanijo et al., 2020; Serge et al., 2020). There is a limitation of the evaluation of the durability of PKS-based concrete materials. This is in terms of its resistance to different aggressive environments such as exposure to chlorides and acids.

Marine systems, ground, drainage systems and other structures that are made from concrete materials  may be exposed to aggressive environments such as chlorides and acids (Balestra, 2020; Kadam et al., 2017; Qu et al., 2021). Therefore, there is a need to investigate the resilience of concrete materials particularly non – traditional concrete such as the PKS-based concrete. Even when subjected to harsh environmental conditions, traditional concrete materials have been found to deteriorate, leading to a compromise in their mechanical and physio-chemical properties. This degradation can ultimately result in diminished resilience over their lifespan (Chikhi, 2024; Kurpińska & Haustein, 2021; Pernicová & Dobiáš, 2016). It is therefore critical to ascertain the durability of PKS-based concrete to the NaCl and H2SO4. Interestingly, other researchers have explored the durability of PKS in concrete, however, these studies used PKS concrete other than coarse aggregates. For instance, Bamaga et al. (2010) examined the chloride resistance of PKS  fuel ash as cementitious material, while  Philip et al. (2019) studied the sulphate attack of PKS fuel ash-based concrete. Additionally, Muthusamy et al. (2018) investigated the sulphate resistance in concrete using PKS as coarse aggregate within a fly ash-based concrete matrix. Both  Muthusamy et al. (2015) and Oti et al. (2015) further explored the sulphate resistance of concrete incorporating palm kernel shell and palm kernel shell ash. Also,  Muthusamy et al. (2015) found the acid resistance of palm kernel ash based concrete to be superior incorporating 20% of the ash.

There is a gap with regard to the performance of palm kernel shell-based concrete exposed to conditions other than ambient and water-cured environments, particularly NaCl and H2SO4 containing surroundings. Therefore, this study seeks to address this gap and contribute to knowledge by expanding the application of this sustainable concrete type to include its durability and resilience in NaCl and H2SO4 containing conditions. With insights into the longevity and mechanical behavior of PKS concrete, these findings could facilitate wider adoption by industry.

# Materials and Methods

## Materials

Commercially available Ordinary Portland Cement with 28th day compressive strength of 42.5 MPa that conforms to the requirements of BS EN 197-1  (British Standards Institution, 2011) was used as cement. River Sand and crushed granite were used as fine and coarse aggregates, respectively. Palm kernel shells used in this study was obtained from a local oil palm production industry in the Bono Region of Ghana. Palm kernel shells were used to replace the coarse aggregates at 0%, 10% and 20% only. Based on past studies and trial mixes where replacement levels varied from 0% to 100%, it was observed that increasing the replacement levels with PKS was accompanied with a decrease in strength. Therefore, this research limited the replacement levels to only 20%. The physical properties of all the aggregates used is presented in Table 1. Before usage the palm kernel shells were thoroughly cleaned and crushed into different sizes. Commercially available Sodium Chloride (NaCl) and sulphuric acid (H2SO4) were used to prepare NaCl and H2SO4 at 5% concentration each. Figure 1 shows the different solutions prepared for exposure of the concrete specimens. The nomenclature of the concrete mixes consisted of letters and numbers, C0 was for the control concrete with zero PKS aggregates. The PK was for the palm kernel-based concrete, followed by numbers 10 and 20 for the 10% and 20% replacement of natural coarse aggregates with PKS aggregates. For example, PK10 represented the PKS-based concrete with 10% replacement of natural coarse aggregates with PKS aggregates.

Figure 1: Prepared NaCl and H2SO4 solutions

Table 1: Physical Properties of aggregates

|  | Fine Aggregates | Coarse Aggregates | PKS |
| --- | --- | --- | --- |
| Maximum Aggregate Size (mm) |  | 14 | 12 |
| Specific Gravity | 2.59 | 2.67 | 1.37 |
| 24-hr Water Absorption (%) | 1 | 0.64 | 18.86 |

## Concrete mixes and casting

A constant concrete mix of 1:2:3 at water cement ratio of 0.6 was used to prepare the concrete. The concrete mix proportion is presented in Table 2. The cement, fine aggregates and water were kept constant while varying the coarse aggregate proportions to fulfil the partial replacement of conventional coarse aggregates with PKS. In this study, the coarse aggregates were used under saturated surface conditions. Concrete was mixed manually. After pouring concrete into the cubes and prism, the specimens were demolded after 24 hours and cured in water until the day of testing. Concrete specimens were exposed to the 5% NaCl solution and 5% H2SO4 solution. After demolding, the specimens were immersed in these solutions for periods of 7, 14, and 28 days, respectively.  Additionally, the compressive strength tests and flexural tensile strength tests were conducted in 100 × 100× 100 mm cube moulds and 100×100×300 mm prisms, respectively. Three specimens were prepared for each characteristic that was evaluated. A total of  81 cubes and 27 prisms were tested in this study.

Table 2: Concrete Mix Proportions and Slump Values

|  | Cement | Fine | Coarse | PKS | Water | Slump | Slump |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Aggregate | Aggregate |  |  | Value | Class |
|  |  | (kg/m3) | (kg/m3) | (kg/m3) | (kg/m3) | (mm) |  |
| C0 | 402 | 804 | 1206 | 0 | 241.2 | 40 | S1 |
| PK10 | 402 | 804 | 1085.4 | 120.6 | 241.2 | 28 | S1 |
| PK20 | 402 | 804 | 964.8 | 241.2 | 241.2 | 12 | S1 |

Testing of physical and mechanical properties

The slump test was conducted in accordance to BS EN 12350-2 (British Standards Institution, 2009) to evaluate the workability of the concrete mixes prepared. Physical property such as the density of the concrete was determined after exposure of the concrete mixes to the different conditions, which was calculated as per BS EN 12390-7 (British Standards Institute, 2000). The compressive and flexural tensile strength tests, were conducted on the procedure given by  BS EN 12390-3 standard (British Standards Institution, 2001) and BS EN 12390-5 (British Standards Institution, 2019), respectively. The density, compressive strength and flexural tensile strength were recorded after 7, 14 and 28 days of curing and exposure to different solutions.

# Results and Discussion

## Slump properties

The slump values of the concrete mixes are presented in Table 2. Based on the test results as shown in Table 2, the slump values were between 10 mm to 40 mm which is classified as low workability according to  BS EN 12350-2 (British Standards Institution, 2009). Among the values obtained the control concrete (C0), is more workable than the other PKS-containing concrete mixes (PK10 and PK20). This is because the PKS materials had a higher water absorption rate than the natural granitic coarse aggregates (see table with physical properties). The high porous nature of PKS aggregates as revealed by (Alengaram et al., 2011) through SEM results, is responsible for its high water absorption rate and hence its lower workability compared to the control (name) concrete. Additionally, with the increase in the PKS aggregates content from 10% to 20%, the concrete mixes became less workable.

Physical and Mechanical Properties

The density, compressive strength and flexural tensile strength of the concrete materials is presented in Figure 2. For the density of the different concrete mixes as shown in Figure 2a, it can be observed that the generally the density of the PKS based concrete was lower than the control concrete without PKS aggregates. Interestingly, the PK10 concrete had higher density values than the PK20 even with the variation in the curing days. Due to the lower specific gravity of the PKS aggregates, the resulting density of the PKS based concrete reduced in comparison to C0 concrete. This is similar to other studies (Acheampong et al., 2018; Ahmad & Yahya, 2016; Philips et al., 2017), which reported lower densities with the replacement of natural aggregates with PKS aggregates. The lower density of PKS-based concrete makes them appropriate for use in lightweight concrete applications where the lower density of concrete is a benefit.

The compressive strength of the different concrete types are presented in Figure 2b. From the experimental results, the control concrete C0 recorded the highest compressive strength of 20.7MPa, 21.3MPa and 25 MPa for the curing period of 7. 14 and 28 days, respectively. These values were higher than the PK10 and PK20 concrete. Among all the varying concrete types, the highest compressive strength was obtained after 28 days of curing. Notably, the C0 specimen was 5.22 % and 30.68% higher than the PK10 and PK20, respectively. Among the PKS based concrete, it is important to note that the PK10 was the optimum concrete for the best compressive strength (23.76MPa) since it had a much lower strength decrease in comparison to the control concrete. Increasing the PKS aggregates content in the concrete was accompanied with a reduction in compressive strength in comparison to the control concrete with no PKS aggregates. Based on experimental results from the slump and density, the reduction in the compressive strength as the PKS aggregates replace the natural aggregates can be related to the low workability and low density in reference to the control concrete. Furthermore, Fanijo et al. (2020) indicates that the physical properties such as the specific gravity and water absorption of the PKS aggregates compromise their mechanical strength when used in concrete production. Although the PKS-based concrete specimens recorded lower compressive strength than the control concrete which is the traditional concrete, it strength was higher than the minimum required strength for concrete which is 17 MPa as per  BS 6073-1 (British Standards Institute, 2002)

For the flexural tensile strength as shown in Figure 2c, the experimental values were taken only after 28 days as curing. The experimental results showed that similar to the compressive strength, the control concrete specimen C0 was the highest followed by the PK10 and then PK20 recorded the least flexural tensile strength. Among the PKS-based concrete specimens, the PK10 which had the highest 28th day flexural tensile strength was 9.08% lower than the C0 and 77.08% higher than PK20. As mentioned earlier, the decreasing flexural tensile strength of the PKS-based concrete specimens is as a result of their physical properties which influences their mechanical properties and hence their flexural tensile strength.

Figure 2: Physical and Mechanical Properties of different concrete types: (a) cube density; (b) compressive strength; (c) flexural strength

## Influence of Concrete to the Varying Exposure Conditions

Experimental results presented in Figure 3 show the change in mass and compressive strength after exposure of the specimens to 5% of NaCl and 5% H2SO4 solutions for 7 days, 14 days and 28 days. From the results presented it can be observed that for the mass change considering the specimens exposed in the 5% NaCl, there was an increase in mass only for the control specimen at 7 days of exposure compared to the water-cured specimens. The other specimens exposed to the 5% NaCl recorded a loss in mass. The specimens which were immersed in the 5% H2SO4 solution on the other hand showed a significant loss in mass. The rate of change in mass is presented in Figure 4a as the percentage change in mass. The degree to which these changes in mass occur is presented, and it can be seen that the mass loss of the specimens in the 5% NaCl was lowest at 0.22% and highest at 0.54%. The specimens immersed in the 5% H2SO4 solutions recorded higher mass losses than those immersed in 5% NaCl. These mass losses were up to 26.65% as the highest mass loss particularly in the palm kernel based concrete.

For the variations in the compressive strengths as depicted in Figures 3b and 4b, there was a general loss in compressive strength regardless of the type of solution that the specimens were immersed in. It is interesting to note that the specimens immersed in the 5% H2SO4 solution recorded higher compressive strength losses compared to those immersed in the 5% NaCl solution. For example, after 28 days of immersion in different solutions, the compressive strength of C0, PK10, and PK20 reduced by 12.8 %, 15.57 %, and 15.28 %, respectively, in 5% NaCl solution compared to the water-cured specimens. In comparison, the compressive strength loss was 55.8 %, 58.42 %, and 59.38 % for the C0, PK10, and PK20 specimens in a 5% H2SO4 solution.

In the absence of chemical investigations to determine the chemical reactions between NaCl and H2SO4 solutions and calcium in concrete materials that cause structural weakness, as indicated by previous research studies (Mahmoodian & Alani, 2017; Wanna et al., 2021), this study relates mass losses to compressive strength loss. It is also widely known from previous studies (Zhang et al., 2022) that reducing the mass (weight) of concrete compromises its mechanical strength properties, as a result of pore formation and weakened strength bonds within the concrete caused by a variety of causative actions. Among the causative action is the exposure of the concrete specimens to NaCl and H2SO4 solutions. The results reveal that when the two distinct types of solutions are at the same concentration, the H2SO4 solution has greater negative effects than the sodium chloride solution. In terms of the influence of the solutions on the various concrete types, the experimental results in Figures 3 and 4 show that the control concrete is more resilient than the palm kernel-based concrete kinds. The findings show that when the two different types of solutions are at the same concentration, the H2SO4 solution has a stronger detrimental impact than the NaCl solution. In terms of how the solutions affect the various concrete types, the experimental results from Figures 3 and 4 show that the control concrete (C0) is more resilient than the palm kernel-based concrete types. This is due to the PKS aggregates' lower physical strength properties compared to natural aggregates, which reduces the mechanical strength of the final concrete. Among the PKS-based concrete specimens, the PK10 was more resilient than the PK20, as shown by the somewhat higher compressive strength drop in the PK20 (59.38%) than the PK10 (58.42 %).  According to (Dousti et al., 2024; Joorabchian, 2010), adding pozzolanic ingredients like metakaolin and fly ash might increase the concrete's resilience to solutions.

(b)

Figure 3: Effect of NaCl and H2SO4 solutions on the different  concrete types: (a) mass ; (b) compressive strength

(a)

(b)

Figure 4: Changes in Physical and Mechanical Properties of different concrete types after exposure to NaCl and H2SO4 solutions: (a) mass ; (b) compressive strength

# Conclusion

The study investigated the effect of palm kernel-based concrete exposed to 5% NaCl and 5% H2SO4 solutions for 7 days, 14 days and 28 days, and compared to the traditional OPC-based concrete as control specimen.  Based on experimental results the following conclusions can be made:

- The traditional concrete exhibited higher density, compressive strength, and flexural strength. However, among the palm kernel-based concrete, the best-performing mix was the one with 10% replacement of natural coarse aggregates.

- All the concrete specimens experienced mass loss when exposed to the solutions.

- H2SO4 solution caused greater mass loss (6.13% to 26.65%) compared to NaCl solution (0.22% to 0.54%)

- The H2SO4 exposure led to a more significant reduction in compressive strength compared to NaCl exposure.

Declaration of Competing Interest

The authors declare that they have no known competing financial interests or personal relationships that could have appeared to influence the work reported in this paper.

Data Availability

The datasets generated during and/or analyzed during the current study are available from the corresponding author on request.

Disclaimer (Artificial intelligence)

Option 1:

Author(s) hereby declare that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc.) and text-to-image generators have been used during the writing or editing of this manuscript.

Option 2:

Author(s) hereby declare that generative AI technologies such as Large Language Models, etc. have been used during the writing or editing of manuscripts. This explanation will include the name, version, model, and source of the generative AI technology and as well as all input prompts provided to the generative AI technology

Details of the AI usage are given below:

1.

2.

3.

# References

Acheampong, A., Ayarkwa, J., Adom-Asamoah, M., & Baiden, B. (2018). Comparative study of the physical properties of palm kernel shells concrete and normal weight concrete in Ghana. https://consensus.app/papers/comparative-study-of-the-physical-properties-of-palm-acheampong-ayarkwa/4983e13976df581e85cd2ca5ee608b0d/

Ahmad, I., & Yahya, K. (2016). The Effect of Oil Palm Shell as Coarse Aggregate Replacement on Densities and Compressive Strength of Concrete Noh. https://consensus.app/papers/the-effect-of-oil-palm-shell-as-coarse-aggregate-ahmad-yahya/ce99c27dc4c258ebbb815672ae3c2e40/

Alengaram, U. J., Mahmud, H., & Jumaat, M. Z. (2011). Enhancement and prediction of modulus of elasticity of palm kernel shell concrete. Materials and Design, 32(4), 2143–2148. https://doi.org/10.1016/j.matdes.2010.11.035

Alqarni, A., Albidah, A., Abbas, H., Almusallam, T., & Al-Salloum, Y. (2022). Concrete Performance Produced Using Recycled Construction and By-Product Industrial Waste Coarse Aggregates. Materials, 15. https://doi.org/10.3390/ma15248985

Alsalami, Z. H. A., Harith, I. K., & Dhahir, M. K. (2018). Utilization of dates palm kernel in high performance concrete. Journal of Building Engineering, 20, 166–172. https://doi.org/10.1016/j.jobe.2018.07.015

Armah, E. A., Koffi, H. A., Sogbey, B. J. A. Y., & Amuzu, J. K. A. (2019). Investigating the Utilization of Ground Palm Kernel Shells for Partial Replacement of Cement in Concrete Using Nondestructive Method. Journal of Modern Materials, 6(1), 1–12. https://doi.org/10.21467/jmm.6.1.1-12

Azunna, S. U. (2019). Compressive strength of concrete with palm kernel shell as a partial replacement for coarse aggregate. SN Applied Sciences, 1(4), 342. https://doi.org/10.1007/s42452-019-0334-6

Balestra, C. E. T. (2020). Service Life and Durability of Reinforced Concrete Structures Present in Marine Environment. In J. M. P. Q. Delgado (Ed.), Building Pathology, Durability and Service Life (pp. 41–55). Springer International Publishing. https://doi.org/10.1007/978-3-030-47302-0_2

Bamaga, S. O., Ismail, M. A., & Hussin, M. W. (2010). Chloride resistance of concrete containing palm oil fuel ash. Concrete Research Letters, 1, 158–166. https://api.semanticscholar.org/CorpusID:138998642

Bediako, M., Gawu, S. K., Adjaottor, A. A., Solomon Ankrah, J., & Atiemo, E. (2016). Analysis of co-fired clay and palm kernel shells as a cementitious material in Ghana. Case Studies in Construction Materials, 5(July), 46–52. https://doi.org/10.1016/j.cscm.2016.06.001

Boateng, E., Kankam, C. K., & Danso, A. K. (2023). Models for Predicting Strength Reduction Factors for Concrete that Utilizes Palm Kernel Shells and Waste Automobile Tires as Aggregates. Journal of Engineering Research and Reports, 24(9), 44–53. https://doi.org/10.9734/jerr/2023/v24i9842

British Standards Institute. (2000). BS EN 12390-7:2000 Testing hardened concrete — Part 7: Density of hardened concrete. BSI Standards Publication, 3(1), 13.

British Standards Institute. (2002). BS 6073 - 1 : 1981 Precast concrete masonry units —Part 1. Specification for precast concrete masonry units. British Standard Publication.

British Standards Institution. (2001). BS EN 12390-3:2001 Testing hardened concrete - Part 3: Compressive strength of test specimens. In BSI Standards Publication (pp. 4–10). file:///C:/Users/hp/Downloads/dlscrib.com-pdf-bs-en-12390-3-dl_b8a9ef69ed054e431ee2df7d05824cb9.pdf

British Standards Institution. (2009). BS EN 12350-2: Testing fresh concrete; Slump test. In BSI Standards Publication.

British Standards Institution. (2011). BS EN 197-1:2011 Composition, specifications and conformity criteria for common cements. BSI Standars Publication.

British Standards Institution. (2019). BS EN 12390-5:2009 Testing hardened concrete — Part 5: Flexural strength of test specimens. BSI Standards Publication, August, 1–22.

Chikhi, A. (2024). Impact of aggressive environments on the mechanical and physico-chemical properties of concrete Impacto de ambientes agressivos nas propriedades mecanicas e fisico-quimicas do concreto Impacto de los entornos agresivos en las propiedades mecanicas y fisic. 1–22. https://doi.org/10.54021/seesv5n2-402

Chinnu, S., Minnu, S., Bahurudeen, A., & Senthilkumar, R. (2021). Recycling of industrial and agricultural wastes as alternative coarse aggregates: A step towards cleaner production of concrete. Construction and Building Materials, 287, 123056. https://doi.org/10.1016/J.CONBUILDMAT.2021.123056

Dousti, A., Saraei, N., Shekarchi, M., & Nikookar, M. (2024). Increasing service life of concrete in sewage treatment plants using silica fume and natural zeolite. Magazine of Concrete Research, 76(8), 375–390. https://doi.org/10.1680/jmacr.23.00129

Fanijo, E., Babafemi, A. J., & Arowojolu, O. (2020). Performance of laterized concrete made with palm kernel shell as replacement for coarse aggregate. Construction and Building Materials, 250, 118829. https://doi.org/10.1016/j.conbuildmat.2020.118829

Fapohunda, C., Kilani, A., Adigo, B., Ajayi, L., Famodimu, B., Oladipupo, O., & Jeje, A. (2021). A Review of Some Agricultural Wastes in Nigeria for Sustainability in the Production of Structural Concrete. Nigerian Journal of Technological Development. https://doi.org/10.4314/njtd.v18i2.1

Gibigaye, M., Godonou, G. F., Katte, R., & Degan, G. (2017). Structured mixture proportioning for oil palm kernel shell concrete. Case Studies in Construction Materials, 6(April), 219–224. https://doi.org/10.1016/j.cscm.2017.04.004

Hamada, H., Jokhio, G., Yahaya, F., Humada, A., & Gul, Y. (2018). The present state of the use of palm oil fuel ash (POFA) in concrete. Construction and Building Materials. https://doi.org/10.1016/J.CONBUILDMAT.2018.03.227

Joorabchian, S. M. (2010). Digital Commons @ Ryerson Durability of concrete exposed to sulfuric acid attack Recommended Citation. https://doi.org/https://doi.org/10.32920/ryerson.14654622.v1.

Kadam, H. P., Desai, D. B., & Gupta, A. K. (2017). A review paper on Deterioration of Concrete in Marine Structures. Imperial Journal of Interdisciplinary Research, 3(2).

Kalisha, S. M., & Munthali, K. (2024). Multi-Factor GIS Modeling for Solid Waste Dumpsite Selection in Lilongwe, Malawi. Sustainability. https://doi.org/10.3390/su16031202

Kim, S.-S., Qudoos, A., Jakhrani, S. H., Lee, J., & Kim, H.-G. (2019). Influence of Coarse Aggregates and Silica Fume on the Mechanical Properties, Durability, and Microstructure of Concrete. Materials, 12. https://doi.org/10.3390/ma12203324

Kumar, S., Smith, S., Fowler, G., Velis, C., Kumar, S., Arya, S., Renã, Kumar, R., & Cheeseman, C. (2017). Challenges and opportunities associated with waste management in India. Royal Society Open Science, 4. https://doi.org/10.1098/rsos.160764

Kurpińska, M., & Haustein, E. (2021). Experimental Study of the Resistance to Influence of Aggressive Liquids on Lightweight Concrete. Materials, 14. https://doi.org/10.3390/ma14154185

Mahmoodian, M., & Alani, A. M. (2017). Effect of Temperature and Acidity of Sulfuric Acid on Concrete Properties. Journal of Materials in Civil Engineering, 29(10), 1–18. https://doi.org/10.1061/(asce)mt.1943-5533.0002002

Muthusamy, K., Fadzil, M. Y., Muhammad Nazrin Akmal, A. Z., Wan Ahmad, S., Nur Azzimah, Z., Mohd Hanafi, H., & Mohamad Hafizuddin, R. (2018). Effect of fly ash content towards Sulphate resistance of oil palm shell lightweight aggregate concrete. IOP Conference Series: Materials Science and Engineering, 342(1). https://doi.org/10.1088/1757-899X/342/1/012105

Muthusamy, Khairunisa, Zamri, N., Mohd Haniffa, I., Sarbini, N. N., & Yahaya, F. M. (2015). Acid Resistance of Oil Palm Shell Lightweight Aggregate Concrete Containing Palm Oil Fuel Ash. Advanced Materials Engineering and Technology III, 754, 326–330. https://doi.org/10.4028/www.scientific.net/AMM.754-755.326

Ogundipe, K. E., Ogunbayo, B. F., Olofinnade, O. M., Amusan, L. M., & Aigbavboa, C. O. (2021). Affordable housing issue: Experimental investigation on properties of eco-friendly lightweight concrete produced from incorporating periwinkle and palm kernel shells. Results in Engineering, 9(August 2020), 0–6. https://doi.org/10.1016/j.rineng.2020.100193

Okina, S. N., Ahouet, L., Taillandier, F., & Ounina, D. (2024). Influence of the Addition of Palm Kernel Shell and Ash on Concrete Performances: Study of Correlations between Intrinsic Material Properties. Advanced Materials Research. https://doi.org/10.4028/p-4wf9hw

Olutoge, F. A., Adesina, A., & Araba, S. T. (2020). Effect of palm kernel shell ash on the strength and durability properties of high-performance concrete. Heliyon, 6(9).

Oti, J. E., Kinuthia, J., Robinson, R., & Davies, P. (2015). The use of palm kernel shell and ash for concrete production. International Science Index, Civil and Environmental Engineering, 9(1), 263–270. https://waset.org/publications/10000699/the-use-of-palm-kernel-shell-and-ash-for-concrete-production

Pernicová, R., & Dobiáš, D. (2016). Resistance of Surface Layers of Concrete against Aggressive Environment. Key Engineering Materials, 722, 44–51. https://doi.org/10.4028/www.scientific.net/KEM.722.44

Philip, J., Ismail, M., & Al-Subari, B. (2019). Strength and sulphate resistance of high performance concrete containing different fineness of Palm oil fuel ash. IOP Conference Series: Materials Science and Engineering, 495. https://doi.org/10.1088/1757-899X/495/1/012100

Philips, E., Mutuku, R., & Mwero, J. (2017). Palm Kernel Shell as Partial Replacement for Normal Weight Aggregate in Concrete. Civil and Environmental Research, 9, 40–47. https://consensus.app/papers/palm-kernel-shell-as-partial-replacement-for-normal-weight-philips-mutuku/5eec35b0f8145a47a2e24319018de3bd/

Qu, F., Li, W., Dong, W., Tam, V. W. Y., & Yu, T. (2021). Durability deterioration of concrete under marine environment from material to structure: A critical review. Journal of Building Engineering, 35, 102074. https://doi.org/https://doi.org/10.1016/j.jobe.2020.102074

Serge, G. N., Didier, F., Gilbert, T., & Evrard, M. (2020). Study of physico-mechanical properties of concretes based on palm kernel shells originating from the locality of Haut Nkam in Cameroon. Journal of Civil Engineering and Construction Technology, 11(1), 13–27. https://doi.org/10.5897/jcect2019.0525

Wanna, S., Pisanu, T., Warangkana, S., & Somnuk, T. (2021). Deterioration in Sulfuric Acid of Cement Pastes incorporating High CaO and Low CaO Fly Ashes. Engineering Journal, 25(2), 71–83. https://doi.org/10.4186/EJ.2021.25.2.71

Zawawi, M. N. A. A., Muthusamy, K., Majeed, A., Musa, R., & Budiea, A. (2020). Mechanical properties of oil palm waste lightweight aggregate concrete with fly ash as fine aggregate replacement. Journal of Building Engineering, 27, 100924. https://doi.org/10.1016/J.JOBE.2019.100924

Zhang, F., Wei, F., Wu, X., Hu, Z., Li, X., & Gao, L. (2022). Study on Concrete Deterioration and Chloride Ion Diffusion Mechanism by Different Aqueous NaCl-MgSO4 Concentrations. Buildings, 12(11). https://doi.org/10.3390/buildings12111843

Kabbo, M. K. I., Sobuz, M. H. R., Aditto, F. S., Khan, M. H., Jabin, J. A., Alahmari, T. S., ... & Khondoker, M. T. H. (2025). Experimental assessment and machine learning quantification of structural eco-cellular lightweight concrete incorporating waste marble powder and silica fume. Journal of Building Engineering, 105, 112557.

Ziamiavaghi, B., & Toufigh, V. (2024). Fracture toughness of alkali-activated concrete subjected to aggressive environment. Construction and Building Materials, 451, 138796.

Magbool, H. M., Zeyad, A. M., Aksaraei, A. M. K., & Johari, M. A. M. (2024). Effect of incorporating ultrafine palm oil fuel ash on the resistance to corrosion of steel bars embedded in high-strength green concrete. Reviews on Advanced Materials Science, 63(1), 20240072.