#### UNDER PEER REVIEW

PERFORMANCE EVALUATION OF A TRICKLIN	G FILTER SYSTEM USING

MODIFIED PALM FRUIT FIBER FOR THE REMOVAL OF CIPROFLOXACIN

#### UNDER PEER REVIEW

##### ABSTRACT

The persistence of pharmaceutical pollutants particularly ciprofloxacin (CIP) in wastewater poses severe environmental and health challenges. The study explores the performance of a trickling filter (TF) system utilizing modified palm fruit fiber (MPFF) as a low-cost and biodegradation packing material for the removal of ciprofloxacin. ). The modified palm fruit fiber was prepared through alkaline to enhance adsorption properties and microbial colonization. Characterization techniques: Fourier transform infrared (FTIR), Scanning electron microscopy (SEM), X-ray fluorescence (XRF)and Thermo-gravimetric analysis (TGA) determines the functional groups, the surface morphology, the elemental composition and the thermal stability of the modified palm fruit fiber respectively. Batch biodegradation was done to determine the effects of contact time, concentration and flow rate in which the optimum percentage removal of 97% was obtained at 9.3hr, 2.6m3/hr and 131.8mg/L. The biodegradation isotherms and kinetics were better fitted with Langmuir and pseudo-second-order models respectively. Under optimized conditions, the experimental percentage removal efficiencies for TSS, TDS and BOD were 83.5%, 47.3% and 32.6% respectively. The biodegradation isotherms and kinetics were better fitted with Langmuir and pseudo-second-order models respectively. The findings demonstrate the potential of modified palm fruit fiber as an environmental friendly alternative to synthetic media in treating pharmaceutical wastewater.

Keywords: Trickling filter, ciprofloxacin, simulated pharmaceutical wastewater, biofilter medium, removal efficiency.

.

#### UNDER PEER REVIEW

##### INTRODUCTION

There were different classes of antibiotics based on their mechanism of action, chemical structure, action spectrum, and route of administration (1). The most common classification of that was based on their mode of action. They include

fluoroquinolones, quinolones, β-lactams, sulfonamides, monobactams, carbapenems, and aminoglycosides. Quinolones (ciprofloxacin, levofloxacin, norfloxacin, and ofloxacin) were

broad-spectrum antibiotics that were widely prescribed (1a). Ciprofloxacin (CIP) was a quinolone antibacterial agent classified as second generation fluoroquinolone with broad-spectrum action that was commonly used to treat human and animal bacterial infections (2) was frequently detected in wastewater due to its widespread use and incomplete removal during conventional treatment processes (3). The presence of CIP or any antibacterial derivative in wastewater and surface water was considered a significant environmental hazard, even at very low concentrations. That was because these products can increase the antibiotic resistance of pathogenic bacteria and generate modifications in the biological balance of aquatic ecosystems (4). The continuous and unregulated discharge of CIP into the aquatic environment posed serious environmental and health problems to man and the aquatic lives. That has resulted in sickness and diseases to mankind and imbalance in the ecosystem and consequently the food chain was threatened. Among the various concerns on humans and environment includes chronic toxicity, endocrine disruption, and direct toxicity of microflora, even at low concentrations. The effect of CIP on the water in a low concentration affects the photosynthesis of plants, transforms the morphological structure of the algae, and then disrupts the aquatic ecosystem (5). When CIP contaminated water was consumed by humans, it might cause anger, nausea, vomiting, headache, diarrhea,

#### UNDER PEER REVIEW

and tremor. The high concentration of CIP can cause severe kidney failure and increase liver and thrombocytopenic enzymes (6).

Several methods have been employed to remove CIP from aqueous solution. They include adsorption in activated carbon (7); zeolites (8); montmorillonites (9); microalgae intake (10); photo catalytic degradation

(11) and electrocoagulation (12); coagulation, sedimentation, biodegradation, photo-transformation, electrochemical, chlorination, ozonation, and Nano filtration through membranes (13;14). There was, therefore, the need to treat the influent streams using eco-friendly and energy efficient methods, prior to discharge into the receiving waters bodies. Trickling filter techniques was simple, reliable, low-cost and effective in treating high

concentrations of organic material. However, most of the treatment techniques that have been employed in the past have the issue of efficiency, generation of toxic by-products, high treatment cost, and high energy requirement, (15). Therefore, efficient and low-cost treatment options that do not introduce harmful by-products were required to eliminate antibiotics from water. Due to the inherent limitations of the existing treatment processes, trickling filters present a good alternative since it is simple, reliable, low-cost, effective in treating high concentrations of organic material, relatively low power requirement and requires moderate skill and technical expertise to operate the system (16;17). A trickling filter was an aerobic wastewater treatment process generally used for industrial effluents and domestic sewage treatment. Its operation consists of passing the effluent to be treated over a fixed bed of support medium. Natural and biodegradable materials have gained attention as alternatives for wastewater treatment. Agricultural residues like palm fruit fiber (PFF), an abundant byproduct in palm oil producing regions, have shown promise due to their porous structure and high surface. The application of palm fruit fiber (PFF) as a support medium instead of the pebbles and other biological fiber used for this purpose was the proposed innovation. The palm fruit fiber offers a great surface for biological film fixation, with very hard fibrous structure. In contact with aqueous solution, the PFF degrades very slowly and can act as a stimulant for the growth of microbes. Modification processes such as alkaline treatment can further enhanced

#### UNDER PEER REVIEW

the adsorption and microbial attachment properties of palm fruit fiber, making it a viable medium for

pharmaceutical pollutant removal in biological systems (18).

The present research work explores the prospect of the preparation of modified palm fruit fiber for the removal of ciprofloxacin from simulated pharmaceutical wastewater using a trickling filter system. The modified adsorbent/biosorbent were investigated by FTIR, SEM, XRF and TGA analysis in detail. Also, the nature of biodegradation was studied by Langmuir and Freundlich isotherm models and the kinetics of biodegradation were investigated in detail. In addition, the percentage removal efficiency was also evaluated.

Biodegradation has long been employed as an adsorption as a conventional method for removing pollutants from water matrices. The biodegradation process's inherent simplicity has made it attractive for tackling CIP contamination (19), (20). Many materials including activated carbon, polymers, rice husks and zeolites have been studied as potential adsorbents. In addition, different nanomaterials and adsorbents have been investigated for their capacity to adsorb CIP from aqueous solutions under different experimental conditions (21), (22), (23), (24).

##### MATERIALS AND METHODS

###### Materials

✔ Palm fruit fiber was sourced from palm fruit bunches after separation of oil and palm kernel from palm fruit from an oil processing facility in Anambra state. ✔ 1000mg (1g) of ciprofloxacin tablet

was dissolved in the 1000 mL standard flask with distilled water, working solutions were prepared from the stock solution and the stock solution was stored in the refrigerator to minimize

degradation and prevent it from losing its integrity.

✔ Sodium hydroxide (NaOH) was used for palm fruit modification.

###### Modification of Palm Fruit Fiber

500g of the PFF would be washed severally in water until there was no oil coming out of the fiber. It would then be treated with 0.5M NaOH for four days at room temperature to remove lignin and hemicellulose, improving its porosity and surface functional groups. After treatment in NaOH, the PFF

would be washed in running water to remove the NaOH and sun dried to obtain fibrous PFF (25) biofilm support medium.

###### Experimental Setup

A bioreactor body with cylindrical shape and made of stainless steel was

constructed. Its length of the reactor would be 152.4 and its diameter would be about 76.2 cm as shown below in fig 1. Modified PFF would be used as filter media in the trickling filter system for microbial growth. The PFF would be placed vertically in a trickling filter system with 129.5 cm in height and diameter varying from 0.5 to 1.0 inches. A distributor would be installed at the top of reactor to spread CIP

#### UNDER PEER REVIEW

wastewater uniformly over filter media. Flow rates would be adjusted with the help of control valves. A 6 inches depth drainage layer would be constructed at the bottom of the reactor for ventilation and for outflow of the wastewater from the reactor tank for final sedimentation. A settling tank would be provided for collecting and settling wastewater. The system was operated at flow rate of 2.6-9.3m3/hr and contact time of 2.6-9.3hr.

#### Fig 1: Schematic diagram of Trickling Filter System setup

###### Analytical Methods

- Total suspended solids were determined through gravimetric analysis

- Total dissolved solids were determined through gravimetric analysis.

- Biological oxygen demand was measured using standard APHA methods (APHA, 2017).

- Characterization of Modified Palm Fruit Fiber: Fourier-transform infrared spectroscopy (FTIR) identified the functional groups responsible for

#### UNDER PEER REVIEW

adsorption. Scanning electron microscopy (SEM) was used to observe surface morphology. X-ray fluorescence (XRF) identified the elemental composition of modified palm fruit fiber while thermo gravimetric analysis (TGA) was to

ascertain thermal stability of modified palm fruit fiber.

###### Performance Evaluation

The removal efficiency was calculated (26) using equation (1)

Removal Efficiency (%) = co-ct/co × 100 (1)

###### Batch Biodegradation Studies

Biodegradation experiments were conducted to evaluate the effect of contact time (2.6hrs-9.3hr), initial ciprofloxacin concentration (131.8-468mg/L) and flow rate (2.6- 9.3m3/hr). The adsorption capacity at the time t (qt (mg/g)) and equilibrium qe (mg/g) was calculated by the following formula (2 ):

qt =co-ct/co × 100 (2)

qe = (co-ce)/m × v (3) where co, ce and ct (mg/l) are model contaminant concentrations at the initial, equilibrium stages and time t, respectively. The adsorbent mass is m (g) and v (mL) is the contaminant solution volume.

    - Biodegradation Isotherm

(27); (28) reported that biodegradation equilibrium isotherms were mathematical models used to describe the equilibrium relationship between the concentration of a pollutant or substrate and its adsorption capacity by microorganisms. These models help characterize how pollutants interact with microbial communities or surfaces at equilibrium, providing insight into the maximum sorption potential, affinity for substrates, and capacity of the system. Isotherms were widely applied in

environmental engineering and microbiology to optimize conditions for

bioremediation, wastewater treatment, and pollutant breakdown in soil or water. The

#### UNDER PEER REVIEW

biodegradation isotherms of the processes were studied using model equations, such as Langmuir and Freundlich. Langmuir biodegradation isotherm model was originally developed by Irving Langmuir in 1916 to describe the dependence of the surface coverage of a degraded solute on adsorbent (29). It was reported to be the most popular model due to its good agreements with sorption experimental data (30)

(31) reported that Langmuir isotherm can be mathematically represented as in equation (32): Q=Qmbce/1+bce (4) Linearizing equ (4) gives equ (5):

Ce/qe=1/KLQm +ce/Qm (5)

Where

Qe=biodegradation capacity at equilibrium (mg/l) Ce=equilibrium concentration of solute (mg/l) Qm=maximum monolayer biodegradation capacity (mg/l) KL=Langmuir isotherm constant (dm3/mg)

Freundlich isotherm was the earliest known relationship describing the non-ideal and reversible adsorption and also not restricted to the formation of monolayer (33). The empirical model has been reported to apply to multilayer adsorption (34) with interaction between degraded molecules (35). It was reported to be most widely used and was applicable to adsorption on heterogeneous surfaces (36) but based on the assumption that the adsorption occurs on heterogeneous sites with non-uniform distribution of energy of adsorption over surfaces (37;38).

Mathematically expressed, Freundlich isotherm was as in equation (6) (39;40):

Qe=KfCe1/n (6)

On linearization, equ (6) becomes equ (7)

#### UNDER PEER REVIEW

lnqe=lnKf + 1/n lnCe (7)

Where

Qe was adsorption capacity at equilibrium (mg/g)

Ce was equilibrium concentration of solute (mg/l) Kf was Freundlich isotherm constant (mg/g)

N was biodegradation intensity

    - Biodegradation Kinetics Studies

Degradation kinetic study was crucial because it affected the stability of pharmaceuticals throughout the stages of product development and testing (41;42). Order of degradation reactions of pharmaceuticals was generally categorized as pseudo-first-order and pseudo-second-order, intra particle diffusion and elovich kinetic model. Kinetic studies provide crucially important information on the time needed for the rate of degradation. If palm fruit fiber was targeted to be used in wastewater facilities, at industrial scales, in addition to its high degrading capacity and removal efficiency,

a high degrading rate was also an essential required characteristic (43). In that study, four kinetic models of pseudo-first order, pseudo-second order, intra particle diffusion and elovich models were selected to evaluate the experimental data.

The pseudo-first order kinetic model indicates rate of degradation was directly correlated to the difference of uptake at concentration and time t, shown as (qe –qt) in the equation (44). The equation was expressed as follows (45;46). A pseudo-first order kinetic equation was given as

Ln(qe-qt)=lnqe-k1t (8) qt: The amount of solute degraded at time t (mg/g). qe:The degradation capacity at equilibrium (mg/g).

k1: rate constant of pseudo-first order degradation model (g/mg/hr)

#### UNDER PEER REVIEW

t: The contact time (hr).

The pseudo-second order kinetic model was known to be successfully applied in systems where the rate controlling was degradation (47), where the removal from a solution was due to physicochemical interactions between the two phases. A pseudo second-order model kinetic equation was given as:

t/qt=1/k2qe2 +1/qt t (9)

Where:

qt = the amount of solute degraded at time t (mg/g) qe = the degradation capacity at equilibrium (mg/g)

k2 = the rate constant of the pseudo-second-order degradation model (g/mg/hr) t = the contact time (hr).

In general, for the degradation process to take place, degrading molecules need to transfer from the bulk phase to the solid surface and then penetrate in the palm fruit fibers pores. Typically diffusing through pores was a slow step. Whether diffusion within the pores was the rate limiting step or not, it can be determined based on intra particle diffusion mode

qt =kdiff t1/2 + C (10)

Where:

qt = the amount of solute degraded at time t (mg/g) C = the intercept

Kdiff = the rate constant of the intra particle diffusion (g/mg/hr)

T1/2 = the half life

#### UNDER PEER REVIEW

The elovich model was first introduced by Elovich (1956) to describe the

biodegradation of solute on solid surfaces. The model was based on the premise that the rate of biodegradation decreases with increasing surface coverage. The model has been extensively adapted for liquid-phase biodegradation, particularly in environmental and industrial contexts. The mathematical expression for the model was given by:

dqt/dt =βe-αqt (11) Integrated equation (11) qt=1/α In(βα×t+1) (12) Where

qt = the amount of solute degraded at time (t) α represents the initial biodegradation rate

β = a constant related to the extent of surface coverage. T = the time

That equation indicated that the adsorption rate was dependent on the amount of solute already degraded.

Rearranging equation (12)

Βαt +1=eαqt (13) Taking the natural logarithm, it results to:

In(qt) =ln(β) + αln(t) (14)

##### RESULTS AND DISCUSSION

  - Characterization of Modified Palm Fruit Fiber

#### UNDER PEER REVIEW

- FTIR Analysis: peaks corresponding alkyene, alkene, alcohol and carboxyl groups were observed confirming successful modification as shown in figure 2a-b.

Fig 2(a-b): FTIR Characteristic of modified palm fruit fiber before and after practical

#### UNDER PEER REVIEW

- SEM Imaging: The modified palm fruit fiber exhibited increased surface roughness and porosity which are crucial for enhanced biodegradation as shown in figure 3a-c.

### Fig 3a: Mag = X1000, W= 12mm at 100μm

Fig 3b: Mag = X900, W =10mm at 150μm

UNDER PEER REVIEW

### Fig 3c: Mag = X800, W = 15mm at 200μm

- X-RF Analysis: The modified palm fruit fiber exhibited elemental composition before and after experiment as showed in table 1 below.

Table 1: XRF Analysis of Modified Palm Fruit Fiber before and after practical

|  | Na2O | MgO | AL2O3 | SiO2 | P2O5 | K2O | CaO | TiO2 | Fe2O3 | MnO |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Palm before | 0.17 | 3.24 | 6.50 | 66.95 | 3.70 | 5.40 | 5.50 | 0.50 | 5.50 | 0.02 |
| Palm after | 0.20 | 3.10 | 6.90 | 66.60 | 3.90 | 5.25 | 5.57 | 0.30 | 5.70 | 0.06 |
| Average | 0.09 | 1.2 | 2.2 | 25.5 | 0.5 | 0.5 | 27.0 | <LD | 6.0 | 0.2 |
| Std. dev | 0.01 | 0.01 | 0.02 | 0.58 | 0.01 | 0.01 | 0.02 | <LD | 0.02 | 0.01 |
| Exp. Value | 2-03 | 4.08 | 8.73 | 25.4 | 1.02 | 2.22 | 26.04 | 0.02 | 13.3 | 1.02 |

- TGA Analysis: The modified palm fruit fiber exhibited decomposition or evaporation of the components within the sample after practical. Mass loss at temperatures exceeding 4000C resulted in (1) charcoal from decomposition

#### UNDER PEER REVIEW

decomposing of residual lignin and (11) more oxidation in the air as shown in figure 4a-b below.

Fig 4 (a-b): TGA graph of Modified Palm Fruit Fiber before and after experiment

#### UNDER PEER REVIEW

###### Batch Biodegradation Studies of the Operating Variables on the Modified Palm Fruit Fiber

    - Effect of Combination of Flow rate and Contact time on TSS, TDS and BOD Removal Efficiency

Flow rate has a significant effect on percentage removal of TSS from simulated pharmaceutical wastewater treatment. As such, the effect of combination of flow rate and contact time on performance evaluation of a trickling filter system using modified palm fruit fiber for removal ciprofloxacin from simulated pharmaceutical wastewater was evaluated using five different flow rates which are 2.6m3/hr, 4m3/hr, 6m3/hr, 8m3/hr and 9.3m3/hr, at concentration of 131.8mg/l, 200mg/L, 300mg/L, 400mg/L and 468mg/L. It could be seen from fig 5a that the highest percentage removal TSS from simulated pharmaceutical wastewater was obtained at flow rate of 2.6m3/hr and concentration of 131.8mg/L. The highest percentage removal of TSS with decrease in flow rate was due to particle agglomeration and filter media performance. Decreased flow rates ensured efficient mass transfer between the liquid phase (wastewater) and solid phase (modified palm fruit fiber) and stopped breakthrough occurrence (48;49;50). Therefore, the percentage removal of TSS obtained at flow rate of 2.6m3/hr at concentration of 131.8mg/L was 99.7%.

The TDS removal of ciprofloxacin from simulated pharmaceutical wastewater was obtained at five different flow rates as shown below in the figure 5b. The flow rates of 2.6m3hr, 4m3hr, 6m3/hr, 8m3/hr and 9.3m3/hr were evaluated at concentration of 131.8mg/l, 200mg/L, 300mg/L, 400mg/L and 468mg/L. There was an increase in TDS percentage removal at 2.6m3/hr and concentration of 131.8mg/L. There was increase in TDS percentage removal as flow rates decreases because it allowed for longer contact times between the water and treatment media, potentially enhancing the removal efficiency of TDS from simulated pharmaceutical wastewater by

#### UNDER PEER REVIEW

development and characterization of modified palm fruit fiber (51; 52). Increased flow rates reduced the efficiency of TDS removal due to shorter contact time between the wastewater and treatment median (modified PFF). However,

excessively low flow rates might lead to issues such as increased residence time in the treatment

system, which could promote bacterial growth or other undesirable reactions (53). Therefore, TDS percentage removal from simulated pharmaceutical wastewater using modified palm fruit fiber at

2.6m3/hr and concentration of 131.8mg/L was 58.7%.

Figure 5c below showed BOD percentage efficiency of ciprofloxacin by application of modified palm fruit fiber (PFF) obtained at optimum flow rates of 2.6m3/hr, 4m3/hr, 6m3/hr, and at concentrations of 131.8mg/L, From the figure, it was observed that there was increase in BOD percentage efficiency as the flow rate decreases during the biodegradation because slower flow rates can allow contact times between the water and treatment media, which enhances the biological degradation of ciprofloxacin and associated organic matter contributing to BOD. Increased flow rates could reduce the efficiency of biological processes due to shorter contact times between the wastewater and microorganisms which could result in lower BOD percentage efficiency as microorganisms have less time to metabolize organic matter, including ciprofloxacin (54; 55; 56). Therefore, the BOD percentage efficiency of ciprofloxacin is 51%.

a

#### UNDER

PEER REVIEW

60

50

BOD Efficiency %

40

30

20

10

0

0 1 2 3 4 5 6 7 Time (hr)

131.8mg/l 200mg/l 300mg/l 400mg/l 468mg/l c

Fig 5 (a-c): Effect of combination of flow rate and contact time for TSS, TDS & BOD removal efficiency from simulated ciprofloxacin pharmaceutical wastewater using modified palm fruit fiber

#### UNDER PEER REVIEW

    - Effect of combination of concentration and contact time on TSS, TDS and BOD Removal Efficiency

Figure 6a below showed the TSS percentage removal by performance evaluation of a trickling filter system using modified palm fruit fiber for removal ciprofloxacin from simulated pharmaceutical wastewater at different concentration of 131.8mg/L, 200mg/L, 300mg/L, 400mg/L and 468mg/L and contact time of 2.6hr, 4hr, 6hr, 8hr and 9.3hr using five different flow rates of 2.6m3/hr, 4m3/hr, 6m3/hr, 8m3/hr and

9.3m3/hr. From the figure 6a below, it could be observed that TSS percentage removal increases as the concentration of simulated pharmaceutical wastewater decreases at flow rates of 2.6m3/hr and concentration of 131.8mg/L respectively because there was less quantity of ciprofloxacin to be removed. Generally, high concentrations of ciprofloxacin could lead to reduced removal efficiency due to saturation of treatment mechanisms or competition with other contaminants for biodegradation sites (50). Therefore, TSS percentage removal is higher at 131.8mg/L which was 97%. The effect of concentration on the removal of TDS by performance evaluation of a trickling filter system using modified palm fruit fiber for removal ciprofloxacin from simulated pharmaceutical wastewater was evaluated using five different

concentrations at different flow rates. The concentrations were 131.8mg/l, 200mg/L, 300mg/L, 400mg/L and 468mg/L at flow rates of 2.6m3/hr, 4m3/hr, 6m3/hr, 8m3/hr and 9.3m3/hr are presented at figure 6b below. There was an increase in TDS percentage removal from simulated pharmaceutical wastewater as the concentration decreased due less competition for reactive sites or biodegradation sites on treatment media (51). Higher concentration of TDS might lead to increased competition for reactive sites or complexation with other ions in the water, which could affect the

mechanisms involved in TDS removal (52; 53). Therefore, the TDS percentage removal of simulated pharmaceutical wastewater was 58.7% at concentration of 131.8mg/l under flow rate of 2.6m3/hr.

#### UNDER PEER REVIEW

###### The effect of concentration on BOD percentage removal of ciprofloxacin during the biodegradation process were evaluated using optimum concentration of 131.8mg/L and optimum flow rate of 2.6m3/hr, 4m3/hr, 6m3/hr.. Figure 6c below showed the effect of concentration in the BOD efficiency of ciprofloxacin by application of modified palm fruit fiber using a trickling filter system. It could be seen from fig 10 that the highest BOD efficiency of ciprofloxacin was obtained at concentration of 131.8mg/L in each of the three flow rates. There was an increase in BOD percentage removal as the conc

entration of ciprofloxacin decreases due to lower concentrations of ciprofloxacin in water could lead to lower levels of organic matter, which may contribute to decreased BOD. That lower organic load can potentially overwhelm biological treatment systems, increasing the percentage of BOD efficiency (54; 55; 56).

## m3/hr

98

96

TSS Removal %

94

92

90

88

86

Time (hr)

0 1 2 3 4 5 6 7

a

#### UNDER PEER REVIEW

131.8mg/l 200mg/l 300mg/l 400mg/l 468mg/l

## 131.8mg/l

60

50

TDS Removal %

40

30

20

10

0	0 1 2 3 4 5 6 7 Time (hr)

2.6m3/hr 4m3/hr 6m3/hr 8m3/hr 9.3m3/hr

b

## 131.8mg/l

60

50

BOD Efficiency %

40

30

20

10

0

Time (hr)

0 1 2 3 4 5 6 7

2.6m3/hr 4m3/hr 6m3/hr 8m3/hr 9.3m3/hr

c

Fig 6 (a-c): Effect of combination of concentration and contact time fot TSS, TDS & BOD removal efficiency from simulated ciprofloxacin pharmaceutical wastewater using modified palm fruit fiber

#### UNDER PEER REVIEW

###### Ciprofloxacin Removal Efficiency

The system achieved an average ciprofloxacin removal efficiency of 97% over a 20- day operational period. The removal mechanism was attributed to a combination of adsorption onto the modified palm fruit fiber and biodegradation by attached biofilms. The results were consistent with the studies utilizing activated carbon, which reported removal efficiencies between 80% and 90% (57).

###### Removal of TSS, TDS and BOD

The trickling filter also demonstrated effective removal of organic and particulate matter:

✔ TSS: 96%

✔ TDS:66%

✔ BOD:50.4%

The high removal rates were attributed to the synergy between biofilm activity and the adsorption properties of modified palm fruit fiber.

###### Biodegradation Isotherm

Equilibrium adsorption isotherm was very useful for the analysis and design of adsorption systems. The equilibrium adsorption experiments were carried out by batch process for different simulated pharmaceutical wastewater concentrations (131.8-468mg/L) at flow rates of 2.6m3/hr, 4m3/hr and 6m3/hr. The adsorption experimental data were plotted for linear isotherm models as shown in figure

11-16 and various isotherm constants were calculated as shown in table 2a-b. The equilibrium adsorption data were analyzed by Langmuir and Freundlich isotherm models. The correlation coefficient determination (R2) showed that the obtained equilibrium data for the optimum flow rate were better fitted to the Langmuir isotherm model than the Freundlich isotherm model. The maximum adsorption values calculated from the Langmuir isotherm model were 2.693, 1.227 and 1.297mg/g at

#### UNDER PEER REVIEW

2.6m3/hr, 4m3/hr and 6m3/hr and at concentrations of 131.8mg/L, 200mg/L and 300mg/L respectively. The essential factor (RL) values were in the range of 0.354, 0.611 and 0.367 at the flow rate of 2.6-6m3/hr and at the concentration of 131.8-300mg/L. The values of 0<RL<1 indicated that the development and characterization of modified palm fruit fiber for simulated pharmaceutical wastewater treatment was favourable at all flow rates. Biodegradation data fit well with Langmuir isotherm, indicating monolayer adsorption with higher coefficient determination (R2) value of 0.9998.

| Response isotherm | Parameters | Flow rate (m3/hrs) | 2.6m3/hrs | 4m3/hrs | 6m3/hrs |
| --- | --- | --- | --- | --- | --- |
| TSS Langmuir | qmax (mg/g) |  | 2.575 | 0.866 | 1.611 |
|  | KL( l/g) |  | 0.027 | 0.150 | 0.050 |
|  | RL |  | 0.593 | 0.207 | 0.440 |

Table 2a: Langmuir isotherm parameters of TSS and TDS and BOD removal from simulated pharmaceutical wastewater at optimum flow rates

|  | R2 |  | 0.9998 | 0.9015 | 0.9288 |
| --- | --- | --- | --- | --- | --- |
| TDS Langmuir | qmax (mg/g) |  | 9.804 | 10.493 | 7.199 |
|  | KL (l/g) |  | 0.0009 | 0.0008 | 0.0013 |
|  | RL |  | 0.904 | 0.914 | 0.867 |
|  | R2 |  | 0.9998 | 0.9818 | 0.9716 |

#### UNDER PEER REVIEW

| BOD Langmuir | qmax (mg/g) |  | 21.505 | 243.902 | 454.545 |
| --- | --- | --- | --- | --- | --- |
|  | KL (l/g) |  | 0.0003 | 0.00002 | 0.00001 |
|  | RL |  | 0.966 | 0.998 | 0.999 |
|  | R2 |  | 0.9999 | 0.9798 | 0.9024 |

| Response isotherm | Parameters | Flow rates (m3/hrs) | 2.6m3/hrs | 4m3/hrs | 6m3/hrs |
| --- | --- | --- | --- | --- | --- |
| TSS Freundlich | Kf (l/g) |  | 239.22 | 2118.85 | 522.40 |
|  | 1/n |  | -0.881 | -1.741 | -1.148 |
|  | R2 |  | 0.9998 | 0.8969 | 0.9298 |
| TDS Freundlich | Kf (l/g) |  | 826.04 | 787.77 | 970.73 |
|  | 1/n |  | -0.4513 | -0.4346 | -0.4904 |
|  | R2 |  | 0.9994 | 0.9805 | 0.9742 |
| BOD Freundlich | Kf (l/g) |  | 491.02 | 391.02 | 375.23 |
|  | 1/n |  | -0.3047 | -0.2336 | -0.2182 |
|  | R2 |  | 0.9993 | 0.9764 | 0.9058 |

Table 2b: Freundlich isotherm parameters of TSS, TDS and BOD removal from simulated pharmaceutical wastewater at optimum flow rates

UNDER PEER REVIEWCe/qe

# TSS at 131.8mg/l

0.5

0.4

0.3

0.1

0

11.4 11.6 11.8 12 12.2 12.4 Ce

2.6m3/hr 4m3/hr 6m3/hr

0.2

a

0.3

0.25

### TDS at 131.8mg/l

#### UNDER PEER

### Ce/qe

0.2

0.15

0.1

0.05

0

34 35 36 37 38 39 40 Ce

2.6m3/hr 4m3/hr 6m3/hr

b

REVIEWCe/qe

0.18 0.16 0.14 0.12 0.1

0.08 0.06 0.04 0.02 0

### BOD at 131.8mg/l

24 25 26 27 28 29 30 Ce

2.6m3/hr 4m3/hr 6m3/hr

c

Fig 7 (a-c): Langmuir biodegradation isotherm for TSS, TDS and BOD percentage removal efficiency

### TSS at 200mg/l

log qe

1.48

1.52

1.5

1.46

1.44

1.42

1.4

1.05 1.055 1.06 1.065 1.07 1.075 1.08 1.085 1.09

### log Ce

2.6m3/hr 4m3/hr 6m3/hr

#### UNDER PEER	REVIEW

1.52 1.53 1.54 log Ce

### log qe

2.265 2.26 2.255 2.25 2.245

2.24 2.235 2.23 2.225 2.22

### TDS at 200mg/l

2.6m3/hr 4m3/hr 6m3/hr

### BOD at 131.8mg/l

log qe

2.275

2.27

2.265

2.26

2.255

1.46 1.47 1.48 1.49 1.5 1.51

2.25

2.245

2.24

1.38 1.4 1.42 1.44 1.46 1.48

### log Ce

2.6m3/hr 4m3/hr 6m3/hr

Fig 8 (a-c): Freundlich biodegradation isotherm for TSS, TDS and BOD percentage removal

###### Biodegradation kinetics Studies

The kinetic data were collected experimentally by passing different concentrations(131.8-468mg/l) of

simulated pharmaceutical wastewater on modified palm fruit fiber at different contact time (2.6-9.3hr), at optimum flow rates (2.6-

#### UNDER PEER REVIEW

6m3/hr) to evaluate the percentage removal of TSS and TDS from simulated pharmaceutical wastewater. To investigate the kinetic models, pseudo-first order, pseudo-second order, intra particle diffusion and elovich kinetic models were used. The kinetic parameters and correlation coefficient determination R2 were listed in table 3a-3b as extracted from the kinetic plot in figure 9-12. The pseudo-second order model fitted the data with correlation coefficient (R2) values of 0.9989, 0.9976, 0.9964 for TSS removal. 0.9988, 0.9988, 0.9972 for TDS removal and 0.8651, 0.8189, 0.9652 for BOD removal.

Table 3a: TSS Biodegradation Kinetic Parameters of Treatment of Simulated Pharmaceutical Wastewater on Modified Palm Fruit Fiber at Conc. Of 131.8mg/L and at optimum Flow rates of 2.6m3/hr, 4m3/hr and 6m3/hr

|  | 131.8mg/L |  |  |
| --- | --- | --- | --- |
| TSS Pseudo-first-order model | 2.6m3/hr | 4m3/hr | 6m3/hr |
| Qt | 3.23 | 8.97 | 1.06 |
| K1 | -0.000046 | -0.00014 | -0.00009 |
| R2 | 0.9349 | 0.9756 | 0.957 |
| TSS Pseudo-second-order model |  |  |  |
| Qt | 0.0003 | 0.0001 | 0.00009 |
| K2 | 0.00037 | 0.00011 | 0.000095 |
| R2 | 0.9989 | 0.9976 | 0.9964 |
| TSS Intraparticle Diffusion model |  |  |  |

#### UNDER PEER REVIEW

| Qt | 0.45 | 0.42 | 1.08 |
| --- | --- | --- | --- |
| Kdiff | 0.0023 | 0.0016 | 0.0038 |
| R2 | 0.9756 | 0.957 | 0.8941 |
| Elovich kinetic model |  |  |  |
| Qt | 0.0796 | 0.0684 | 0.0691 |
| Α | 0.043 | 0.03 | 0.0291 |
| R2 | 0.8699 | 0.9532 | 0.9278 |

Table 3b: TDS Biodegradation Kinetic Parameters of Treatment of Simulated Pharmaceutical Wastewater on Modified Palm Fruit Fiber at Conc. of 131.8mg/L and at optimum Flow rates of 2.6m3/hr, 4m3/hr and 6m3/hr

|  | 131.8mg/L |  |  |
| --- | --- | --- | --- |
| TDS Pseudo-first-order model | 2.6m3/hr | 4m3/hr | 6m3/hr |
| Qt | 2.21 | 2.93 | 3.39 |
| K1 | -0.000115 | -0.000115 | -0.000115 |
| R2 | 0.9875 | 0.9575 | 0.9623 |
| TDS Pseudo-second-order model |  |  |  |
| Qt | 0.051 | 0.055 | 0.054 |

| K1 | 0.0076 | 0.0068 | 0.0058 |
| --- | --- | --- | --- |
| R2 | 0.9988 | 0.9988 | 0.9972 |
| TDS Intraparticle Diffusion model |  |  |  |
| Qt | 1.067 | 1.375 | 1.741 |
| Kdiff | 0.0052 | 0.0052 | 0.0058 |
| R2 | 0.9958 | 0.9923 | 0.9725 |

UNDER PEER REVIEW

| Elovich kinetic model |  |  |  |
| --- | --- | --- | --- |
| Qt | 0.2355 | 0.2631 | 0.2711 |
| Α | 0.1238 | 0.1201 | 0.1149 |
| R2 | 0.9673 | 0.9504 | 0.9155 |

Table 3c: BOD Linear Kinetic Parameters for the removal of Ciprofloxacin from Simulated CIP Pharmaceutical Wastewater by Application of Modified Palm Fruit Fiber at 131.8mg/L, 200mg/L and 300mg/L

|  | 131.8mg/l |  |  |
| --- | --- | --- | --- |
| BOD Pseudo-first order | 2.6m3/hr | 4m3/hr | 6m3/hr |
| Qt | 1.184 | 1.570 | 1.373 |
| K1 | -0.00016 | -0.000115 | -0.000115 |

| R2 | 0.8651 | 0.8189 | 0.9652 |
| --- | --- | --- | --- |
| BOD Pseudo-second order |  |  |  |
| Qt | 0.012 | 0.015 | 0.015 |
| K2 | 0.0023 | 0.0026 | 0.0024 |
| R2 | 0.9894 | 0.9918 | 0.9973 |
| BOD Intra particle diffusion |  |  |  |
| Qt | 0.939 | 0.958 | 1.150 |

UNDER PEER REVIEW

| Kdiff | 0.0047 | 0.0036 | 0.0038 |
| --- | --- | --- | --- |
| R2 | 0.8651 | 0.8189 | 0.9652 |
| Elovich kinetic model |  |  |  |
| Qt | 0.168 | 0.196 | 0.199 |
| Α | 0.087 | 0.09 | 0.085 |
| R2 | 0.7536 | 0.712 | 0.9302 |

UNDER PEER	REVIEWln(qe-qt)

0 2 4 6 8 10 Time (t) hr

2.6m3/hr 4m3/hr 6m3/hr

0.889 0.888 0.887 0.886 0.885 0.884

0.883 0.882 0.881

### TSS at 131.8mg/l

(a)

3.9987

3.9986

### ln(qe-qt)

3.9985

3.9984

3.9983

3.9982

### TDS at 131.8mg/l

3.9981

0 2 4 6 8 10 Time(t) hr

2.6m3/hr 4m3/hr 6m3/hr

(b)

UNDER PEER	REVIEWln(qe-qt)

3.5917 3.5916 3.5915 3.5914 3.5913

3.5912 3.5911

# BOD at 131.8mg/l

0 2 4 6 8 10 Time (t) hr

2.6m3/hr 4m3/hr 6m3/hr

3.591 3.5909

c

Fig 9 (a-c): Biodegradation Pseudo-first order Kinetic Model of TSS, TDS & BOD removal efficiency at optimum Flow rates.

# TSS at 131.8mg/l

(a)

300

250

t/qt

200

150

100

50

0

0 2 4 6 8 10 Time (t) hr

2.6m3/hr 4m3/hr 6m3/hr

UNDER PEER REVIEWt/qt

### TDS at 131.6mg/l

70

60

50

40

30

20

10

0

0 2 4 6 8 10 Time (t) hr

(b)

### BOD at 131.8mg/l

(c)

100

90

80

70

### t/qt

60

50

40

30

20

10

0

0 2 4 6 8 10 Time (t) hr

2.6m3/hr 4m3/hr 6m3/hr

Fig 10 (a-c): Biodegradation Pseudo-second order Kinetic Model of TSS, TDS & BOD removal efficiency at optimum Flow rates

UNDER PEER REVIEW

### qt

0.06 0.05 0.04 0.03 0.02 0.01 0

### TSS at 131.8mg/l

0 1 2 3 4 5 t1/2

2.6m3/hr 4m3/hr 6m3/hr

a

### TDS at 131.8mg/l

0.16

0.155

0.15

### qt

0.145

0.14

0.135

0.13

b

0.125

0 1 2 3 4 5 t1/2

2.6m3/hr 4m3/hr 6m3/hr

#### UNDER PEER REVIEWqt

0.14 0.12 0.1

0.08 0.06 0.04 0.02 0

### BOD at 131.8mg/l

0 1 2 3 4 5 t1/2

2.6m3/hr 4m3/hr 6m3/hr

c

Fig 11 (a-c) TSS, TDS and BOD Biodegradation Intra particle Diffussion Kinetic Model of Treatment of Simulated Pharmaceutical Wastewater on Modified Palm Fruit Fiber at optimum Flow rates

(a)

0.06

0.05

0.04

### qt

0.03

0.02

0.01

### TSS at 131.8mg/l

0

0 1 2 3 4 5 t1/2

2.6m3/hr 4m3/hr 6m3/hr

#### UNDER PEER REVIEWqt

0.16 0.155 0.15 0.145 0.14 0.135 0.13

0.125

### TDS at 131.8mg/l

t1/2

2.6m3/hr 4m3/hr 6m3/hr

0 1 2 3 4 5

b

0.14

0.12

0.1

### qt

0.08

0.06

0.04

c

### BOD at 131.8mg/l

0.02

0

0 0.5 1 1.5 2 2.5 lnt

2.6m3/hr 4m3/hr 6m3/hr

Fig 12 (a-c) TSS, TDS and BOD Biodegradation Elovich Kinetic Model of Treatment of Simulated Pharmaceutical Wastewater on Modified Palm Fruit Fiber at optimum Flow rates

#### UNDER PEER REVIEW

###### Comparison with Synthetic Media

Modified palm fruit fiber showed comparable pollutant removal efficiency to synthetic media, with the added advantages of biodegradation, lower cost, and reduced environmental impact. That makes it a sustainable alternative for regions with abundant palm fruit fiber waste.

##### CONCLUSION

The study demonstrates the potential of modified palm fruit fiber as a cost-effective and sustainable packing materials for the removal of ciprofloxacin in trickling filter systems. The system showed high removal efficiencies for CIP, TSS and TDS and slightly lower of BOD, suggesting its viability for treating pharmaceutical-laden wastewater. Future studies should focus on scaling up the system and investigating the long-term stability of modified palm fruit fiber.

##### DISCLAIMER

Author (s) hereby declare that NO generative AI technologies and text-to image generators have been used during writing or editing of manuscripts.

##### REFERENCE

  - IlurdozDe, M.S., Sadhwani, J.J., & Reboso, J.V. (2022)a. Antibiotic removal processes from water & wastewater for the protection of the aquatic environment - a review,” Journal of Water Process Engineering, 45, article 102474.

#### UNDER PEER REVIEW

  - IlurdozDe, M.S., Sadhwani, J.J., & Reboso, J.V. (2022)b. Antibiotic removal processes from water & wastewater for the protection of the aquatic environment - a review,” Journal of Water Process Engineering, 45, article 102474.

  - Mezni, M., Saied, T., Horri, N., & Srasra, E. (2017). Removal of enrofloxacin from aqueous solutions using illite and synthetic zeolite X, Surf. Eng. Appl. Electrochem., 53, 89–97.

  - Kummerer, K. (2016). Pharmaceuticals in the Environment: Sources, Fate, Effects, and Risks. Springer-Verlag Berlin Heidelberg

  - El-Shafey, E.S.I., Al-Lawati, H., & Al-Sumri, A.S. (2012). Ciprofloxacin adsorption from aqueous solution onto chemically prepared carbon from date palm leaflets, J. Environ. Sci., 24, 1579–1586.

  - Samadi, M.T., Shokoohi, R., & Harati, R., (2015). Evaluation of Synthesized Fe3O4/MWCNTs Nanocomposite Used in the Heterogeneous Fenton Process for the Removal of Ciprofloxacin Antibiotic. J. Water Wastewater., (5): 80-89.

  - Yoosefian, M., Ahmadzadeh, S., Aghasi, M., & Dolatabadi, M. (2016). Optimization of electrocoagulation process for efficient removal of ciprofloxacin antibiotic using iron electrode; kinetic and isotherm studies of adsorption. J. Mol. Liq., 225: 544-553.

  - Ahmed, M.J. (2017). Adsorption of quinolone, tetracycline, and penicillin antibiotics from aqueous solution using activated carbons: review, Environ. Toxicol. Pharmacol., 50 (2017) 1–10.

  - Zide, D., Fatoki, O., Oputu, O., Opeolu, B., Nelana, S., & Olatunji, O. (2018). Zeolite ‘adsorption’ capacities in aqueous acidic media; the role of acid choice and quantification method on ciprofloxacin removal, Microporous Mesoporous Mater., 255, 226–241.

  - Wang, C.J., Li, Z.H., & Jiang, W.T. (2011). Adsorption of ciprofloxacin on 2:1 dioctahedral clay minerals, Appl. Clay Sci., 54, 723–728.

  - Xiong, J.Q., Kurade, M.B., & Jeon, B.H. (2018). Can microalgae remove pharmaceutical contaminants from water?, Trends Biotechnol., 36, 30–44

#### UNDER PEER REVIEW

  - Gharaghani, M.A., & Malakootian, M. (2017). Photocatalytic degradation of the antibiotic ciprofloxacin by ZnO nanoparticles immobilized on a glass plate, Desal. Wat. Treat., 89, 304–314.

  - Yoosefian, M., Ahmadzadeh, S., Aghasi, M., & Dolatabadi, M. (2016). Optimization of electrocoagulation process for efficient removal of ciprofloxacin antibiotic using iron electrode; kinetic and isotherm studies of adsorption. J. Mol. Liq., 225: 544-553.

  - Sharma, N., & Dhiman, N. (2017). Kinetic and thermodynamic studies for ciprofloxacin hydrochloride adsorption from aqueous solution on CuO nanoparticles, Int. J. ChemTech Res., 10, 98–106.

  - Ding, R., Zhang, P.F., Seredych, M., & Bandosz, T.G. (2012). Removal of antibiotics from water using sewage sludge- and waste oil sludge-derived adsorbents, Water Res., 90, 40–6.

  - Balarak, D., Baniasadi, M., Lee, S ., & Joon, M. (2021). Ciprofloxacin adsorption onto Azolla

filiculoides activated carbon from aqueous solutions,” Desalination and Water Treatment, 218, 444–453.

  - Arami, M., Limaee, N.Y., Mahmood, N. M., & Tabrizi, N. S. (2006). Equilibrium and Kinetics Studies for the adsorption of direct and acid dyes from aqueous solution by soy meal hull: Journal of Harzardous Materials 135, 171-176

  - Kaya, G.G., Aznar, E., & Deveci, H. (2021). Low-cost silica xerogels as potential adsorbents for ciprofloxacin removal, Sustainable Chemistry and Pharmacy, 22, 100483.

- Ghosh, S., Othmani, A., Malloum, A., Christ, O.K., Onyeka, H., Alkafaas, S.S., Nnaji, N.D.,Bornman, C., Al-sharify, Z.T., Ahmad, S., Dehyhani, M.H., Mubarak, N.M.,Tyayi, I., Karri, R.R., Koduru, J.R., & Suhas. (2022). Removal of mercury from industrial effluents by adsorption and advanced oxidation processes: A comprehensive review, J. Mol. Liq. vol. 367.

- Al-Buriahi, A.K., Al-sharbani, M.M., Radinmohamed, R.M.S., Al-gheethi, A.A., Sharma, A., & Ismail, N. (2022). Ciprofloxacin removal from non-clinlcal environment: A critical review of current methods and future trend prospects, J. Water Process Eng. vol. 47

- Das, S., Barui, A., & Adak, A. (2020). Montmorillonite impregnated electrospun cellulose acetate nanofiber sorptive membrane for ciprofloxacin removal from wastewater, J. Water Process Eng. vol. 37

- Veclani, D., & Melchior, A. (2020). Adsorption of ciprofloxacin on carbon nanotubes: Insights from molecular dynamics simulations, J. Mol. Liq. vol. 298

- Bo, X., Sun, J., Mei, Q., Wei, B., An, Z., Qiu, Z., Han, D., Xie, J., & He, M. (2021). Theoretical insights into the degradation of tyrosol simulated by hydroxyl and sulfate radicals in wastewater and ecotoxicity evaluation, J. Clean. Prod. vol. 293

- Igwegbe, C.A., Oba, S.N., Aniagor, C.O., Adeniyi, A.G., & Ighalo, J.O. (2021). Adsorption of ciprofloxacin from water: A comprehensive review, J. Ind. Eng. Chem. vol. 93, pages 57-77

- Chowdhury, S., Mishira, R., Saha, P., & Kushwaha, P. (2011). Adsorption thermodynamics, kinetics and isosteric heat of adsorption of malachite green onto chemically modified rice husk. Desalination, 265, 159-168

- Adesanya, T. M. (2021). “Utilization of Agricultural Waste in Wastewater Treatment: A Review”.

Journal of Environmental Engineering, 147 (5):04021035.

- Demirbas, A. (2008). Heavy metal adsorption onto agro-based waste materials: A review Journal of Hazardous Materials, 157, 220-229

#### UNDER PEER REVIEW

28 .Hameed, B. H. & Foo, K. Y. (2010). Insights into the modelling of an adsorption isotherm

systems. Chemical Engineering Journal, 15,2-10

- Patel, P. M. (2005). Supercritical Fluid Extraction of Rice Bran with Adsorption on Rice Hull Ash. PhD Dissertation, Louisiana State University, Louisiana, USA

- Khare, P. (2011). Treatment of phenolic water using adsorption. M. Tech Thesis, National Institute of Technology, Rourkela, India

- Hameed, B. H. & Foo, K. Y. (2010). Insights into the modelling of an adsorption isotherm system. Chemical Engineering Journal, 15,2-10

- Soto, M. L., Moure, A., Dominguez, H. & Parajo, J. C. (2011). Recovery, concentration and purification of phenolic compounds by adsorption: A review. Journal of Food Engineering Safety, 71, 274-283

- Hameed, B. H., & Foo, K. Y. (2010). Insights into the modelling of adsorption isotherm systems. Chemical Engineering Journal, 156, 2-10

- Gayatri, S. L & Ahmaruzzaman, M. D. (2010). Adsorptive Technology for the removal of phenolic compounds from wastewater using low-cost adsorbent. Asian University Journal of Science and Technology, 5(2), 156-166

- Khare, P. (2011)b. Treatment of phenolic water using adsorption. M. Tech Thesis, National Institute of Technology, Rourkela, India

- Mohd-din, A. T., Hameed,B. H. & Ahmad, A. L., (2009). Batch adsorption of phenol onto a physicochemical-activated coconut shell. Journal of Hazardous Materials, 161, 1522-1529

- Gulipalli, CH,. Prasad, B., & Wasewa, I.K. (2011). Batch study, equilibrium and kinetics of adsorption of selenium using rice husk ash (RHA). Journal of Engineering Science and Technology, 6(5), 586-605

- Kadhim, F. & Al-Seroury, F. A. (2012). Characterization of the removal of phenol from aqueous solution in fluidized bed column by rich husk adsorbent. Research Journal of Recent Sciences, 1, 145-151

- Albadarin, A. B., Yang, Z., Mangwandi, C., Glocheux, Y., Walker, G. & Ahmad, M.N.M. (2013).

Experimental design and batch experiments for

#### UNDER PEER REVIEW

optimization of Cr (VI) removal from aqueous solutions by hydrous Cerium oxide nanoparticles. Chemical Engineering Research and Design, http://dx.doi.org/10.1016/j.cherd. 2013.10.015

- .Rohman, A., Windarsih, A., Lukitaningsih, E., Rafi, M., Betania, K., & Fadzillah, N. A. (2020).

The use of FTIR and Raman spectroscopy in combination with chemometrics for analysis of biomolecules in biomedical fluids: A review. Biomed. Spectrosc. Imaging. (8): 55-7

- José, A. G., Belkis, C. S., Erick, R. B., & Jorge, R. (2019). Adsorption and kinetic studies of the removal of ciprofloxacin from aqueous solutions by diatomaceous earth, Desalination and Water Treatment, 162 (2019) 331–340.

- Nasseri, S., Mahvi, A.H., Seyedsalehi, M., Yaghmaeian, K., Nabizadeh, R., Alimohammadi, M., & Safari, G.H. (2017). Degradation kinetics of tetracycline in aqueous solutions using peroxydisulfate activated by ultrasound irradiation: effect of radical scavenger and water matrix, J. Mol. Liq., 241, 704–714.

- Mutasim, E.E., Maathir, A.A., Rashida, M.H., & Mawia, H.E. (2017). Removal of Ciprofloxacin Hydrochloride from Aqueous Solution by Pomegranate Peel Grown in Alziedab Agricultural Scheme - River Nile State, Sudan. Advances in Biochemistry. 5 (5), 89-96.

- Ho, S. Y. & Mckay, G. (2004). Sorption of copper (11) from aqueous solution by peat. Water, Air and Soil Pollution, 158,77-97

- Demirbas, A. (2009). Agricultural based activated carbons for the removal of	dyes from aqueous solutions: A review. Journal of Hazardous Materials, 167, 1-9

- Ho, S. Y. and Mckay, G. (2004). Sorption of copper (11) from aqueous solution by peat. Water, Air and Soil Pollution, 158,77-97

- Abhang, R. M., Kumar, D. & Darakar, S. V. (2011). Design of photo catalytic reactor for degradation of phenol in wastewater.

- Al-Taweel, S. S. & Saud, H. R. (2016). “Route for synthesis of pure anatase TiO2 nanoparticles via ultrasound assisted Sol-gel method”.

#### UNDER PEER REVIEW

- Ali, T., Tripathin, P., Azam, A., Raza, W., Ahmed, A. S., Ahmed, A. & Muneer, M. (2017). “Photocatalytic performance of doped TiO2 nanoparticle under visible –light irradiation”.

- Mautner, A., Reischer, G., Genser, J., Kirschner, A., Baranyi, C., Blaschke, A. P., & Farnleither,

  - H. (2019). Hydraulic conditions influence faecal inductor organisms released from riverbed sediments during flood events. Water Research, 155, 253-265.

- Quan, X., Liu, Y., Xiong, J., Chen, S., Zhao, H., Zeng, Z., & Zhao, Y. (2018). The removal of ciprofloxacin in water by activated carbon: Kinetics, equilibrium and effects of solution chemistry. Chemosphere, 191, 801-809.

- Lee, S., Seo, D., Ra, K., & Hong, S. (2017). Effects of hydraulic conditions on the removal of

dissolved organic matter and disinfection byproduct formation potential in coagulation processes. Journal of Water Process Engineering, 19, 209-217.

- Kang, J., Kim, S., Lee, Y., & Lee, H. (2016). Effects of hydraulic retention time on the performance and microbial community of anaerobic ammonium oxidation (Anammox) process. Bioresource technology, 200, 840-846

- Hu, J., Sun, Y., Xie, S, Liu, R., Zhang, K., Ma, F., & Zhao, G. (2021). Effects of hydraulic retention time on the performance and microbial community of anaerobic ammonia oxidation process. Journal of Environmental Chemical Engineering.

- Dlugosz, M., Cichosz, M. & Bialoweic, A. (2019).” Influence of hydraulic retention time on efficiency of nitrogen compounds removal and biogas production in the anaerobic digestion of nitrogen-rich substrate.” Chemical engineering journal, 356, 433-440.

- Tang, Z., Shan, Z., Cui, H., Wang, Y., Zhang, X., & Liang, X. (2019). Enhanced removal of ciprofloxacin by the carbonized leaves of water caltrap under ultraviolet irradiation: performance and mechanism. Chemical Engineering journal, 360, 201-208.

#### UNDER PEER REVIEW

- Quan, X., Liu, Y., Xiong, J., Chen, S., Zhao, H., Zeng, Z., & Zhao, Y. (2018). The removal of ciprofloxacin in water by activated carbon: Kinetics, equilibrium and effects of solution chemistry. Chemosphere, 191, 801-809.

- Xie, Y., Wang, D., Li, G., Sun, J., & Wang, Y. (2019). “Mechanisms and kinetics of the removal of ciprofloxacin from aqueous solution by a low-cost adsorbent-bamboo biochar”. RSC Advances, 9 (22), 12599-12610.

- Sun, J., Zhang, L., Zhand, M., Cao, Z., Wu, J., Xie, Y., & Wang, Y. (2020). Removal of ciprofloxacin from aqueous solution using polyethylenemine modified sugar bagasse: Kinetics, isotherm and mechanism studies. Chemical engineering journal, 385, 123959.

- Radjenovic, J., Petrovic, M., Ventura, F., & Barcelo, D. (2008). Rejection of pharmaceutical in nanofiltration and reverse osmosis membrane drinking water treatment. Water Research, 42 (13), 3601-3610.

- Kummerer, K. (2009). Antibiotics in the aquatic environmemt- A review part 1. Chemosphere, 75 (4), 417-434.

- Huggett, D. B., Khan, I. A., Ansari, M. I., Khan, S, A., Chisliti, K. A. & Shakil, S. (2003). Fluoroquinolone antibiotics in the environment. Journal of Environmental Science and Health, part B, 38 (1), 41-49.

- Roosta, M., Ghaedi, M., Shokri, N., Daneshfar, A., Sahraei, R. & Asghari, A. (2014). Optimization of the combined ultrasonic assisted/ adsorption method for the removal of malachite green by gold nanoparticles loaded on activated carbon: Experimental design. Spectrochimica Acta A: Molecular and Biomolecular Spectroscopy, 118, 55-65

- Nguyen, T.T., Dang, V.B.H., Dang, V.H., Vo, Q.T., Nguyen, T.T., & Nguyen, V.T. (2024). Electrochemical treatment of textile wastewater using electrodes from pyrolyzed rice husks. Desalination water treat, 320

- Li, F., Xie, Z., Wen, J., Tang, T., Jiang, L.,& Hu, G. (2023). Synthesis of cellulose poly (Acrylic Acid) using sugarcane bagasse extracted cellulose fibers for the removal of heavy metal ions. Int. J. Mol. Sci, 24 (10), p. 8922

- Arshad, R., Javed, T., & Thumma, A. (2023). Exploring the efficiency of sodium alginate beads and cedrus deodara sawdust for adsorptive removal of crystal violet dye. J. Dispers Sci. Technol, pp. 1-14

- Shah, A., Zakharova, J., Batool, M., & Coley, M.P. (2024). Removal of cadmium and zinc from water using sewage sludge-derived biochar

- Shah, A., Arjunan, A., Thumma, A., Zakharoka, J., Balarinwa, T., Devi, S., & Batool, M. (2024). Adsorptive removal of arsenic from drinking water using KOH-modified sewage sludge-derived biochar

- Moradi, O., Hossinian, A., Kakee, M., & Mirklan, S. (2023). The effect of sustainable applications of chitin and chitosan to remove dyed pollutants using adsorption: A review. Nano, 18 (14), Article 2330006

- Ghzal, O., Javed, T., & Batool, M. (2023). Potentially of easily prepared low-cost rice husk biochar and burnt clay composite for removal of methylene blue dye from contaminated water. Environmental Science: Water Rsearch and Technology.

- Rehman, H., Javed, T., Thumma, A., Uddin, A. N., Singh, N., & Baigi, M.M. (2024). Potential of easily available low-cost raw cotton for the elimination of methylene blue dye from polluted water. Desalination Water Treat, Article 100319

- Aljeboree, A.M., Salah, O.H., Karim, M.M., Alsaadi, S., Jawad, M.A., & Alkaim, A. F. (2024). Synthesis and characterization of acrylamide-based graft poly (Acrylic Acid) hydrogel nanocomposite for methylene blue dye removal and investigation isotherm models

- Sudn, S., Kaushal, J.,& Khajuria, A. (2024). Efficient adsorption of anionic dye (congo red) using copper-carbon dots doped magnetic biochar: Kinetic, isothermal, and regeneration studies. Clean Technol Environ Policy, 26 (2), pp. 481-497.

- Dube, N., Smolarze, K., Sokowski, A., Sweizak, J., Qverjordet, I.B., Ellingsen, I., Wielogorska, S., Sqrensen, L., Walecka, D.,& Kwasniewski, S. (2024). Human pharmaceuticals in the

artic-A review. Chemosphere, 364, Article 143172, 10.1016/j. Chemosphere. 143172

- Deng, J., Zhang, W., Zhang, L., Qin, C., Wang, H., & Ling, W. (2024). Micro-interfacial behavior of antibiotic resistant bacteria and antibiotic resistance genes in the soil environment: A review. Environ. Int.., 191, article 108972, 10.1016/j. Envint. 2024.108972

- Rathod, P.B., Singh, M.P., Taware, A.S., Deshmukk, S.U., Tagad, C.K., Kulkarni, A., & Kanagare, A, B. (2024). Comprehensive insights into water remediation: chemical, biotechnological, and nanotechnological perspectives. Environ. Pollut. Bioavailability, (36)., Article 2329660, 10.1080/26395940.2024.2329660