Review Article

SUPERABSORBENT POLYMER COATING ON SEEDS: A REVIEW

The growing impacts of climate change such as unpredictable weather patterns, prolonged droughts, and extreme heatwaves pose serious threats to global agriculture by reducing crop productivity and endangering farmers’ livelihoods. In regions like India, where drought stress is frequent, there is an urgent need for climate-resilient agricultural practices. One promising solution is the use of Superabsorbent Polymers (SAPs) in seed coatings. These hydrophilic materials can absorb and retain large amounts of water, creating a moisture-rich micro-environment that supports seed germination and early seedling development under water-limited conditions. SAPs function through osmotic pressure and are available in fossil-based and bio-based, degradable and non-degradable forms. With growing concerns about environmental sustainability, bio-based and biodegradable SAPs are gaining popularity. Various SAP formulations such as cross-linked polyacrylamide and starch-graft polymers have shown positive effects on crops like maize, cotton, red clover, and others, enhancing water-use efficiency, nutrient uptake, and drought tolerance. Despite their benefits, challenges remain, including high costs, limited biodegradability of synthetic SAPs, and reduced performance in extreme soil and climate conditions. Ongoing research should focus on developing cost-effective, biodegradable alternatives and evaluating their long-term field performance to support sustainable agricultural systems.

ABSTRACT

Keywords:

Climate-resilient agriculture, Superabsorbent polymers, Seed coating, Drought tolerance, Water retention, Bio-based SAPs, Germination improvement, Sustainable farming, Biodegradable hydrogels, Soil moisture management

- INTRODUCTION

Climate change has led to unpredictable shifts in weather patterns, resulting in more frequent and severe droughts, floods, and heatwaves. These extreme weather events are severely impacting crop yields, threatening farmers' livelihoods and the availability of food. In recent years, India has faced significant drought stress, underscoring the need for developing climate-resilient strategies to mitigate crop losses. To combat water stress in arid and semi-arid regions, several seed treatment techniques can be employed, such as seed priming, hardening, and coating seeds with water-absorbing materials. One promising method is the use of Superabsorbent Polymers (SAP), which provide a moisture-rich environment for seeds during stress conditions. Besides its water retention capabilities, SAP aids in seed germination, seedling growth, and promotes sustainable agriculture. Recently, bio-based SAP has gained significant attention in agriculture due to its effectiveness and eco-friendly properties.

Superabsorbent Polymer (SAP)

SAP are a group of hydrophilic materials capable of absorbing and retaining a significant amount of water in their structure (Zohuriaan-Mehr et al., 2008). These polymers are composed of flexible polymer chains forming a three-dimensional network with loosely arranged cross-links, and bearing dissociated ionic functional groups (Ahmed, 2015). The ability of hydrogels to absorb water is due to the hydrophilic groups attached to the polymeric backbone, while the gel's dissolution is prevented by the addition of a cross-linker.

The genesis of SAPs in agriculture can be traced back to the United States Department of Agriculture (USDA), which developed the first SAP in 1980. This innovation, marketed under the trademark of “Super Slurper”, marked a pivotal moment in applying polymer technology to  agricultural challenges, which further inspires further research into SAPs application in farming. 
although SAPs gained widespread attention in the 1980s, their evolution began earlier with the development of fiber-based water-absorbing materials in the 1960s.  By 2015, global SAP production had grown substantially (Chen et al., 2021), highlighting their expending usage not only in agriculture by also in hygiene products, medical equipments, and industrial applications.
The continued advancement of SAPs has led to the development  of polycondensate-type SAPs in 2017 and cross-linked acrylic homopolymers in 2018. These innovations enhanced SAPs’ water retention and absorption capacity, making them more effective and efficient for use in agricultural use. The ongoing improvement of SAPs reflects the continued efforts to advance water management and promote agricultural sustainability.

Structure and mechanism of SAPs

SAPs’ structure consists of hydrophilic polymer chains containing functional groups with strong affinity for water. These chains are interconnected via cross-linking units, and both the type and concentration of cross-linkers significantly influence the gel’s overall absorption and swelling capcity. The polymer network typically contains negatively charged functional groups, primarily carboxylate ions (–COO-), which repel one another and induce expansion of the polymer chains. The positively charged ions, such as sodium (Na+) or potassium (K+), help maintain electrostatic balance within the network.

The absorption mechanism of SAPs is driven by osmotic pressure, and their distinctive properties arise from their high hydrophilicity and the presence of hydrophilic groups and a well-cross-linked structure (Zohuriaan et al., 2009).

The polymer backbone is hydrophilic due to the presence of water-attracting carboxylic acid groups (-COOH). When these polymers come into contact with water, a range of interactions, such as hydration and hydrogen bonding, occur between water molecules and polymer chains?. Hydration results from the attraction of  polar water molecules to ionized groups, including   -COO⁻ and their associated cations, Na⁺ or K⁺ ions, while hydrogen bonding increases the water retention. These interactions, combined with hydrogen bonding between the polymer and water molecules, increase the system's entropy, making the polymer dissolve in water. Therefore to prevent complete dissolution of the polymer in water, cross-linking is introduced to restrict polymer chain mobility? To prevent deformation? To increase SAPs’ durability?

Most synthetic SAPs are polyelectrolyte gels, containing ionic groups that dissociate in water. This dissociation leads to an overall charge density along the polymer chains and an increase in the concentration of mobile ions within the gel. These mobile ions contribute to the osmotic pressure within the gel, which along with electrostatic repulsion between polymer chains, this allows SAPS to absorb substantial amount of water. The high-water absorbency of SAPs results primarily from the osmotic pressure difference between the swollen gel and the surrounding solution, as well as the repulsive forces between polymer chains caused by the ionic groups.

The water absorption capacity of SAPs can be modified by changing the ratio of ionic to non-ionic components within the polymer network. For example, incorporating non-ionic acrylamide to poly(sodium acrylate) can alter the water absorption properties of the polymer (Zhu, 2015).

Fig 1: Structure of Superabsorbent Polymer

Table 1. Applications of Superabsorbent polymer

| Applications | Description | References |
| --- | --- | --- |
| Agriculture | Enhances water retention in the soil, slows down irrigation frequency, promotes plant growth | Chirino et al., 2011 |
| Horticulture | Increases germination and seedling establishment through preservation of root zone moisture | Dorraji et al., 2010 |
| Diapers and Hygiene Products | Used in baby diapers, adult incontinence products, and sanitary napkins for absorbing fluids | Buchholz & Graham, 1998 |
| Medical Applications | Used in wound dressings and surgical pads to absorb exudate and promote healing | Ahmed, 2015 |
| Construction | Poured into concrete to hold water for curing, minimize cracking and shrinkage | Jensen & Hansen, 2001 |
| Waste Management | Absorbs toxic liquids in industrial waste for safe disposal | Ekebafe et al., 2011 |
| Cleanup of Oil Spill | Oil or organic solvents can be absorbed by modified SAPs for environmental cleanup | Kabiri et al., 2003 |

Classification of SAP

Fossil-Based and Bio-Based SAPs: Environmental Aspects

SAPs are classified on their origin and biodegradability, with the primary distinction being between fossil-based and bio-based SAPs. This classification is important to determine the environmental sustainability and overall impact of such materials to ecological systems?. Fossil-based SAPs are synthesized from non-renewable sources, such as petroleum, whereas bio-based SAPs are derived from renewable sources, including plants and microorganisms. The selection between fossil-based and bio-based SAPs is application-dependent and is guided by the consideration of  environmental impact (Chen et al., 2022).

Fossil-based SAPs are typically produced from monomers such as methacrylic acid, acrylamide, and acrylic acid. These polymers are usually non-biodegradable and do not naturally decompose in the environment which leads to their long-term persistence in the soil and water. The accumulation of these material can cause environmental contamination and possibly harming ecosystems and have adverse effects on soil fertility, water quality, and diversity. Moreover,  the degradation of fossil-based SAPs has been linked to microplastic formation, and raised additional concerns regarding their infiltration into the food web and also potential impacts on human health.

In contrast, bio-based SAPs have gained more popularity due to their biocompatibility, non-toxicity, and biodegradability (Dispat et al., 2020). These bio-based SAPs are synthesized from renewable material sources such as starch, cellulose, chitosan, and alginate, which provide a more environmentally friendly alternative to petroleum-based polymers. Bio-based SAPs are designed to degrade naturally with the over time, thereby reducing  environmental impact and less possibility of pollution. The byproducts of their biodegradation are generally harmless and can be reintegrated back into the environment without damage. The application of bio-based SAPs is consistent with the increasing interest in minimizing the environmental impact of farming and ensuring a circular economy.

Degradable vs. Non-Degradable SAPs: Effect on Soil and Water

Degradability of SAPs is another key parameter in assessing their environmental burden and sustainability. Biodegradable SAPs undergo natural decomposition over time, reducing their environmental footprint. Meanwhile, non-degradable SAPs have a tendency to remain in the environment, necessitating additional waste management strategies. Degradability of a SAP depends upon its chemical composition, molecular weight, and the presence of degradable linkages within the polymer backbone.

Non-degradable SAPs, typically derived from fossil-based polymers, can accumulate in the soil and water, leading to long-term environmental pollution. The persistence of these polymers can disrupt soil structure, reduce water infiltration, and inhibit plant growth. Furthermore, non-degradable SAPs can break down into microplastics, which can contaminate water sources and pose risks to aquatic life and human health. The disposal of non-degradable SAPs often requires energy-intensive methods such as incineration or landfilling, which add to environmental contamination.

Degradable SAPs present a greener alternative. These materials are formulated to degrade into smaller molecules via processes like hydrolysis, oxidation, and biodegradation. The products of degradation are normally non-toxic and can be reused by the environment without any adverse effects. For example, the biodegradability of graft-starch-polyacrylate SAPs can be evaluated using α-amylase, an enzyme that hydrolyses starch via hydrolysis process (Dispat et al., 2020). The method involves subjecting the SAP to α-amylase, and monitoring the release of hydrolysis products over time. The quantity of released hydrolysis products is an indicator of the degradation rate and mechanism. Through the production and application of degradable SAPs, one can reduce the environmental footprint of these products and enhance more environmentally friendly farming practices.

Types of SAPs used in seed coating

Common SAPs employed in seed coating include cross-linked potassium polyacrylate (PAL), cross-linked polyacrylamide-based polymer (PAM), PAM with graphite (PAM+G) (Amirkhani et al., 2023), and starch-graft-2-Propenoic acid (potassium salt) (STR) (Dispat et al., 2020). These materials are selected based on their functional properties, especially their ability to enhance water retention, seed germination, and seed establishment. Additionally, the SAPs performance formulations can vary in terms of water absorbency and flowability. The selection of an appropriate SAP depends on multiple factors, including cost, availability, the desired level of water retention, and environmental considerations (Amirkhani et al., 2023). The selection of the appropriate SAP type is crucial for optimizing the performance of seed coatings. Additionally, specific crop types, soil conditions, and climate should be considered to ensure optimal performance?. Tailoring the SAP type to  specific application, not only maximize the benefits of seed coating but also contribute to sustainable agricultural practices.

Techniques for Uniform SAP Application

The effectiveness of SAPs in seed coating largely depends on the uniformity of their application. Consistent and adequate amount of SAP coating is crucial for maximizing the benefits of enhanced water retention and improved germination. Various coating techniques are employed to ensure uniform coverage and adherence, each with its advantages and limitations, varying from simple manual methods to sophisticated industrial processes, depending on the scale of application and the desired level of precision.

One common method involves direct application of SAPs powder to the seeds, followed by the addition of a binding agent to ensure adherence. The seeds are then  thoroughly mixed to achieve relatively even coating. This method is relatively simple and cost-effective, making it suitable for small-scale applications. However, it may not provide the most uniform coverage, and the amount of SAP applied can be difficult to control precisely.

Alternatively, SAPs can be applied in the form of a solution or slurry by  dissolving the SAP in water or another suitable solvent Where the seeds are then immersed in this solution or sprayed with it, allowing the SAP to coat their surface. This method can provide more uniform coverage than powder application, as the liquid SAP can penetrate into the crevices and irregularities of the seed surface. The concentration of the SAP solution and the duration of exposure can be adjusted to control SAPs deposition. After coating, the seeds are typically dried to remove excess moisture and solidify the coating.

Amirkhani et al. (2023) developed a seed coating method that resulted in the uniform application of SAP from seed to seed. This method involves using a rotating drum or fluidized bed coater to apply the SAP to the seeds in a controlled manner. The seeds are placed in the coater, and the SAP is sprayed onto them as they are being mixed. The rotating drum or fluidized bed ensures that the seeds are constantly moving, allowing the SAP to coat their surface evenly. This method can provide highly uniform coverage and precise control over the amount of SAP applied.

Seed Coating vs. Planting Groove Application

The application of SAPs in agriculture is not limited to seed coating, they can also be applied directly to the planting grooves or soil. Each method offers distinct advantages depending on the crop, soil conditions, and water management practices. Barros et al. (2017) evaluated the effects of SAP applied as a seed coat and within planting grooves on the initial development of sorghum seedlings under water deficit conditions. Their findings indicated that both methods increased the growth of aerial parts for sorghum seedlings, suggesting that SAPs can be effective regardless of the application method.

Seed coating involves applying a thin layer of SAP directly to the seed surface, forming a localized water reservoir around the seed. This method is particularly beneficial in promoting germination and early seedling establishment, as the SAP provides a readily available source of moisture during the critical stages of development. Additionally, seed coating is also a cost-effective way to deliver SAPs, as it requires a relatively small amount of material per seed.

Conversely, planting groove application involves depositing the SAP directly into the furrow or groove where the seeds are planted. This method can provide a larger volume of water to the developing seedlings, which may be advantageous in extremely dry conditions or for crops with high water requirements. Planting groove application can also improve soil structure and water infiltration in the immediate vicinity of the roots. However, the higher SAP volume required per unit area increases application costs compared to seed coating.

Adireddy et al. (2024) explored different application methods of indigenous hydrogels, including seed treatment, slurry application, and soil application, on crop yield and water productivity in a soybean-wheat cropping system. They found that seed treatment and slurry application of superabsorbent polymer hydrogel improved system productivity and water productivity, highlighting the effectiveness of these methods in enhancing crop performance.

Emerging Application Methods: Slurry and Soil Application

In addition to seed coating and planting groove application, emerging methods such as slurry and soil application are gaining attention for their potential to enhance the effectiveness of SAPs in agriculture. Slurry application involves mixing the SAP with water to create a slurry that is then applied to the seeds or soil. This method can provide a more uniform distribution of SAP compared to dry application, as the slurry can penetrate into the soil pores and coat the seed surface more effectively (Guilherme et al., 2015).

Slurry application can be particularly advantageous for improving soil moisture retention and reducing water loss through evaporation. Upon absorbing water, the SAP forms a gel-like substance that bind the soil particles together, increasing its water-holding capacity. This can reduce the need for frequent irrigation and improve crop yields, especially in water-limited environments. Additionally, slurry application can also be used to deliver other beneficial substances to the soil, such as fertilizers and micronutrients, further enhancing crop growth.

Meanwhile soil application involves incorporating the SAP directly into the soil surrounding the seeds or plants. This method can improve soil structure, water infiltration, and nutrient availability, creating a more favourable environment for root growth. Soil application can be particularly beneficial in sandy soils, which have low water-holding capacity and are prone to nutrient leaching. The SAP in the soil absorbs water and nutrients, preventing them from being lost through drainage and making them available to the plants as needed.

Adireddy et al. (2024) found that seed treatment and slurry application of superabsorbent polymer hydrogel improved system productivity and water productivity in a soybean-wheat cropping system. This suggests that these emerging application methods can be effective in enhancing crop performance and promoting sustainable agriculture. Further research is needed to optimize these methods and determine their suitability for different crops, soil types, and climate conditions.

Effects of SAP Seed Coatings on Major Crops

Maize: Enhanced Growth and Emergence Parameters

Maize, a global staple crop, has been the center of various studies that investigate the impact of SAP seed coatings. These studies consistently demonstrate the potential of SAPs to enhance maize yields, especially under water-stressed conditions. Ondreikov et al. (2023) reported that SAP-coated maize seeds had better growth and emergence traits than untreated controls. The SAP coating ensured that there was sufficient moisture surrounding the seeds, resulting in quicker and more even germination.

SAP-coated maize seeds were noted by the researchers to have increased germination, faster emergence time, and higher seedling vigor when compared to the control. These improvements were attributed to the SAPs’ ability to retain and gradually release water, thereby supporting seedling development even under arid or suboptimal irrigation conditions.

Tao et al. (2018) synthesized SAPs based on carbohydrates and evaluated their impact on germination potential and seedling growth of maize. They reported that a suitable level of SAPs could enhance root length, shoot length, germination rate, and total biomass. The SAPs based on carbohydrates were effective in holding water and releasing it slowly to growing seedlings, making a consistent supply of moisture available. The enhanced shoot length and root length noted in the SAP-treated maize plants indicate that the SAPs also increased nutrient absorption and plant growth.

Cotton: Increased Seedling Emergence Under Water Stress

Cotton, a fiber crop of significant commercial importance, is usually cultivated under dryland conditions and is drought-stress sensitive. Cotton seedling establishment is important for realizing high yields, but it is difficult in water-deficit conditions. Panayiota Papastylianou and Angeliki Kousta (2020) investigated the effects of Zeba, a corn starch-based polymer, on cotton seedling emergence under water stress. The findings indicated that Zeba stimulated seedling emergence and enhanced root and shoot characteristics, and thus SAPs may prove to be an effective solution for water conservation in cotton.

Zeba-treated seeds under the same stress conditions demonstrated a significantly faster rate of emergence and a shorter time to emergence than untreated seeds.  By keeping the area around the seeds sufficiently moist, the SAP treatment encouraged germination and the early growth of seedlings.  Increased water and nutrient uptake may have been facilitated by the SAP, as evidenced by the improvements in root and shoot parameters.

It is found that SAPs might prove to be a useful means of enhancing cotton yield in dryland fields. By offering an easily accessible supply of water to the sprouting seeds, SAPs can eliminate the problems of water stress and facilitate successful seedling establishment. This can result in increased yield and better returns for the cotton growers.

Other Crops: Red Clover, Caragana, Milk Thistle, and More

SAP seed coatings have also been tested on a number of other crops such as red clover, Caragana korshinskii, milk thistle, barley and fenugreek, and peppermint. These investigations have mostly reported beneficial impacts of SAPs on germination, plant growth, and drought resistance, reflecting the widespread utility of this technology. Amirkhani et al. (2023) discovered that SAP-coated red clover seeds exhibited higher germination in the laboratory and better stand establishment under field conditions, largely due to the ability of the SAP coating to maintain suitable moisture levels around the seeds. This moisture availability promoted more rapid and uniform germination, even under variable environmental conditions..

Su et al. (2017) examined the impact of SAPs on the survival and growth of Caragana korshinskii, a drought-tolerant shrub employed in soil conservation and afforestation. It was established that SAP application greatly enhanced seedling growth and survival of Caragana under drought stress conditions As the SAPs ensured that water was conserved in the soil and was available as an easily accessible source of moisture for seedlings developing.

Moghadam et al. (2019) analyzed the influence of SAPs on germination and growth of milk thistle, a medicinal crop with a variety of potential health benefits. They observed that SAP treatment enhanced the germination rate, seedling vigor, and biomass of milk thistle. SAPs ensured proper moisture levels around the seeds and seedlings, facilitating faster and better growth.

Ali et al. (2023) examined the impact of SAPs on barley and fenugreek seedling emergence in sandy soil. They established that SAP treatment boosted the GI for both plants. They also noted that WGE values were greater in instances where SAP had been applied, suggesting that SAPs can significantly contribute to the conservation of moisture for seed germination in sandy soil.

Sepehri et al. (2023) studied the effects of SAPs on the growth and yield of peppermint, an aromatic herb used for flavouring and medicinal purposes. They found that SAP application increased the plant height, leaf area, and essential oil content of peppermint due to the SAPs ability to retain water in the soil, providing a consistent moisture supply for the developing plants.

These studies illustrate the general applicability of SAP seed coatings for enhancing crop yields across a range of environments. Through the provision of an easily accessible source of water to germinating seeds and young seedlings, SAPs may facilitate the surmounting of water stress issues and the resultant successful establishment of crops. This can result in increased yields, enhanced economic profitability, and increased sustainability of farming practices.

Benefits of Superabsorbent Polymer Seed Coating

The benefits of SAPs seed coating can be summarised in Table 1 as follows:

| SAPs Benefits |  | Details | References |  |
| --- | --- | --- | --- | --- |
| Improved Germination & Seedling Establishment | - Enhances seed germination rate and seedling vigor, especially under water stress. - Increases emergence percentage and reduces mean emergence time. - Promotes better early growth, coleoptile, and root development. |  |  | Dolatkordestani et al. (2023); Amirkhani et al. (2023); Ondreikov et al. (2023); Papastylianou & Kousta (2020) |
| Improved Water Use Efficiency | - Retains and gradually releases water to seeds and seedlings. - Enhances moisture conservation, especially in sandy soils. - Improves system water productivity and reduces water loss via evaporation or seepage. |  |  | Patra et al. (2022); Ali et al. (2023); Adireddy et al. (2024) |
| Mitigation of Drought Stress | - Acts as a water buffer during drought periods. - Improves plant growth, chlorophyll content, and yield under water deficit. - Reduces oxidative stress by lowering antioxidant enzyme activity and proline content. | Guan et al. (2014); Dolatkordestani et al. (2023); Naderi et al. (2023) |
| Enhanced Nutrient Uptake | - Encapsulates fertilizers for controlled release. - Enhances nutrient use efficiency and reduces leaching. - Increases grain and stover yield when used with humic acid and fertilizers. - Improves macronutrient absorption in plants. | Rajamani et al. (2021) |

Limitations of SAPs

The limitations of SAPs application is summarised in Table 2 as follows:

| Limitation | Details | References |
| --- | --- | --- |
| Environmental Concerns |  | - Many SAPs are petroleum-based and non-biodegradable. - Contribute to microplastic accumulation, soil and water contamination. - Long-term use can harm soil structure, reduce infiltration, and inhibit plant growth. - Need for biodegradable alternatives to prevent ecological damage. | Dingley et al. (2024) |  |
| Cost and Availability |  | - High production costs limit accessibility for small-scale farmers in developing countries. - Limited availability of specialized SAP formulations. - Cost and supply constraints reduce adoption despite agronomic benefits. - Research is needed to improve affordability and local access. | Dingley et al. (2024) |  |
| Performance |  | - High temperatures accelerate SAP degradation; cold conditions delay water absorption and release. - SAP effectiveness decreases in highly acidic, alkaline, or saline soils. - Soil pH and salinity sensitivity restricts use in diverse environments. - May be unsuitable for extreme climate or soil conditions without formulation adaptation. | Liao et al. (2016) |  |

- CONCLUSION

Superabsorbent polymer seed coating is a promising technology for enhancing seed germination, promoting plant growth, and mitigating drought stress, especially in arid and semi-arid regions. By creating a localized water reservoir around the seed, SAPs ensure a consistent moisture supply during the critical germination and early seedling stages. Studies have shown that SAP seed coatings can improve germination rates, seedling vigour, and overall plant performance in a variety of crops, including maize, cotton, red clover, and milk thistle. Furthermore, SAPs can be used in conjunction with fungicides without compromising their protective effects. To ensure the sustainable use of SAPs, it is important to consider their environmental impact, optimize their formulation and application rate, and explore the use of alternative water sources. Future research should focus on developing novel, biodegradable SAPs, investigating their interactions with other seed treatments, and conducting long-term field studies to assess their sustainability under different agricultural management practices.

REFERENCES

Adireddy, R.G., Manna, S., Patanjali, N., Singh, A., Dass, A., Mahanta, D., & Singh, V.K. (2024). Unveiling superabsorbent hydrogels efficacy through modified agronomic practices in soybean–wheat system under semi‐arid regions of South Asia. Journal of Agronomy and Crop Science, 210(4), 12730. https://doi.org/10.1111/jac.12730

Ahmed, E.M. (2015). Hydrogel: Preparation, characterization, and applications: A review. Journal of Advanced Research, 6(2), 105–121.

Ali, R.R., Nassar, I.N., Ghallab, A., Ali, E.F., Alqubaie, A.I., Rady, M.M., & Awad, A.A. (2023). Alleviation of water-deficit stress on seed germination of barley and fenugreek in a sandy soil using superabsorbent polymer. Agronomy, 13(9), 2324. https://doi.org/10.3390/agronomy13092324

Amirkhani, M., Mayton, H., Loos, M., & Taylor, A. (2023). Development of superabsorbent polymer (SAP) seed coating technology to enhance germination and stand establishment in red clover cover crop. Agronomy, 13(2), 438. https://doi.org/10.3390/agronomy13020438

Buchholz, F. L., & Graham, A. T. (1998). Modern Superabsorbent Polymer Technology. Wiley.

de Barros, A.F., Pimentel, L.D., Araujo, E.F., de Macedo, L.R., Martinez, H.E.P., Batista, V.A.P., & da Paixão, M.Q. (2017). Super absorbent polymer application in seeds and planting furrow: It will be a new opportunity for rainfed agriculture. Semina: Ciências Agrárias, 38(4), 1703–1714. https://doi.org/10.5433/1679-0359.2017v38n4p1703

Chen, J., Wu, J., Raffa, P., Picchioni, F., & Koning, C.E. (2022). Superabsorbent polymers: From long-established, microplastics generating systems, to sustainable, biodegradable and future proof alternatives. Progress in Polymer Science, 125, 101475.

Chirino, E., Vilagrosa, A., Vallejo, V.R. (2011). Using hydrogel and clay to improve the water status of seedlings for dryland restoration. Plant Soil, 344(1-2), 99-110. http://dx.doi.org/10.1007/s11104-011-0730-1

Dorraji, S. S., Golchin, A., & Ahmadi, S. (2010). The effects of hydrophilic polymer and soil salinity on water holding capacity and growth of lettuce. Soil Use and Management, 26(2), 198–203.

Dingley, C., Cass, P., Adhikari, B., & Daver, F. (2024). Application of superabsorbent natural polymers in agriculture. Polymers from Renewable Resources, 15(2), 210–255. https://doi.org/10.1177/20412479231226166

Dispat, N., Poompradub, S., & Kiatkamjornwong, S. (2020). Synthesis of ZnO/SiO2-modified starch-graft-polyacrylate superabsorbent polymer for agricultural application. Carbohydrate Polymers, 249, 116862.

Dolatkordestani, M., Taghvaei, M., & Mastinu, A. (2023). Effective treatments for the successful establishment of Milkweed (Calotropis procera L.) under water deficit. Land, 12(11), 1987. https://doi.org/10.3390/land12111987

Ekebafe, L. O., Ogbeifun, D. E., & Okieimen, F. E. (2011). Polymer applications in agriculture. Biokemistri, 23(2), 81–89.

Guan, Y., Cui, H., Ma, W., Zheng, Y., Tian, Y., & Hu, J. (2014). An enhanced drought‐tolerant method using SA‐loaded PAMPS polymer materials applied on tobacco pelleted seeds. Scientific World Journal, 2014, 752658. https://doi.org/10.1155/2014/752658

Guilherme, M.R., Aouada, F.A., Fajardo, A.R., Martins, A.F., Paulino, A.T., Davi, M.F., Rubira, A.F. and Muniz, E.C. (2015). Superabsorbent hydrogels based on polysaccharides for application in agriculture as soil conditioner and nutrient carrier: A review. European Polymer Journal, 72, 365-385.

Jensen, O. M., & Hansen, P. F. (2001). Water-entrained cement-based materials: I. Principles and theoretical background. Cement and Concrete Research, 31(4), 647–654

Kabiri, K., Omidian, H., Zohuriaan-Mehr, M. J., & Doroudiani, S. (2003). A novel approach for preparation of highly oleophilic superabsorbent polymers. Journal of Macromolecular Science, Part B: Physics, 42(6), 1111–1120. https://doi.org/10.1002/pat.356

Liao, R., Wu, W., Ren, S., & Yang, P. (2016). Effects of superabsorbent polymers on the hydraulic parameters and water retention properties of soil. Journal of Nanomaterials, 2016, 5403976. https://doi.org/10.1155/2016/5403976

Ebrahimi Moghadam, H., Taghvaei, M., Sadeghi, H., & Zarei, M. (2019). Effect of organic coats with superabsorbent polymers on improving the germination and early vigor of Milk thistle (Silybum marianum L.) seeds under salinity stress. Desert, 24(2), 207–215. https://doi.org/10.22059/JDESERT.2019.76361

Naderi, R., Afranjeh, E., Heidari, B., Emam, Y., & Egan, T.P. (2023). Salicylic acid and superabsorbent polymers could alleviate water deficit stress in camelina (Camelina sativa L.). Communications in Soil Science and Plant Analysis, 54(20), 2863–2873. https://doi.org/10.1080/00103624.2023.2245408

Papastylianou, P., & Kousta, A. (2020). Effect of superabsorbent polymer on seedling emergence and growth of cotton under water stress conditions. Academic Press, pp. 85–91. https://doi.org/10.15835/buasvmcn-hort:2020.0011

Patra, S.K., Poddar, R., Brestic, M., Acharjee, P.U., Bhattacharya, P., Sengupta, S., Pal, P., Bam, N., Biswas, B., Barek, V., & Ondrisik, P. (2022). Prospects of hydrogels in agriculture for enhancing crop and water productivity under water deficit condition. International Journal of Polymer Science, 2022, 4914836. https://doi.org/10.1155/2022/4914836

Rajamani, K., Reddy, K.I., & Srinivas, A. (2021). Influence of super absorbent polymer and humic acid on maize yield and nutrient uptake on rainfed alfisols. International Journal of Environment and Climate Change, 11, 97–106. https://doi.org/10.9734/ijecc/2021/v11i1230559

Sepehri, S., Abdoli, S., Asgari Lajayer, B., Astatkie, T., & Price, G.W. (2023). Changes in phytochemical properties and water use efficiency of peppermint (Mentha piperita L.) using superabsorbent polymer under drought stress. Scientific Reports, 13(1), 21989. https://doi.org/10.1038/s41598-023-49452-z

Su, L.Q., Li, J.G., Xue, H., & Wang, X.F. (2017). Super absorbent polymer seed coatings promote seed germination and seedling growth of Caragana korshinskii in drought. Journal of Zhejiang University Science B, 18(8), 696–706. https://doi.org/10.1631/jzus.B1600350

Tao, J., Zhang, W., Liang, L., & Lei, Z. (2018). Effects of eco-friendly carbohydrate-based superabsorbent polymers on seed germination and seedling growth of maize. Royal Society Open Science, 5(2), 171184. https://doi.org/10.1098/rsos.171184

Zhu, Q., Barney, C.W., & Erk, K.A. (2015). Effect of ionic crosslinking on the swelling and mechanical response of model superabsorbent polymer hydrogels for internally cured concrete. Materials and Structures, 48, 2261–2276.

Zohuriaan‐Mehr, M.J., Pourjavadi, A., Salimi, H., & Kurdtabar, M. (2009). Protein‐ and homopoly(amino acid)-based hydrogels with super‐swelling properties. Polymer Advanced Technologies, 20(8), 655–671.