Review Article

Silk Sericin Nanomaterials: A Sustainable Frontier in Advanced Biomedical and Cosmetic Applications

ABSTRACT

Sericin, a hydrophilic protein derived from silkworm cocoons, is emerging as a multifunctional biomaterial with significant potential in biomedical and cosmetic applications. Its unique properties, including biocompatibility, biodegradability, antioxidant capacity, and moisture retention, have led to increased interest in its utilization, particularly in nanotechnology-driven formulations aimed at enhancing therapeutic and cosmetic efficacy while maintaining environmental sustainability. In biomedical contexts, sericin has demonstrated promise in drug delivery systems, wound healing materials, and scaffolds for tissue engineering, where its bioactivity aids cellular proliferation, collagen deposition, and controlled drug release. In cosmetics, sericin contributes to hydration, anti-aging, and skin-whitening effects, aligning with consumer demand for natural, eco-friendly skincare solutions. The integration of sericin with nanotechnology has further advanced its application potential by facilitating improved bioavailability, controlled release, and enhanced stability of active ingredients. This review critically examines recent advancements in the extraction, characterization, and application of sericin-based nanomaterials in biomedical and cosmetic sectors, addressing the mechanisms underpinning their efficacy, challenges in scalability and regulatory pathways, and future research prospects for their development as sustainable materials within the bioeconomy. The insights presented aim to guide researchers and industry stakeholders in harnessing sericin’s properties to advance next-generation healthcare and skincare innovations, thereby contributing to circular economy goals while promoting human health and wellness.

Keywords: Sericin, nanotechnology, biomaterials, cosmeceuticals, drug delivery, wound healing, sustainability

- INTRODUCTION

Sericin is a hydrophilic, globular silk protein that constitutes approximately 20–30% of the silk cocoon and is traditionally removed during degumming in sericulture (Figure 1) [1,2,3]. This removal process has historically contributed to environmental pollution, yet sericin’s inherent bioactivity has increasingly attracted interest for high-value biomedical and cosmetic applications [4,5]. Its amino acid composition, rich in serine, aspartic acid, and glycine, contributes to its excellent moisture-retention, film-forming ability, and biocompatibility [6]. Additionally, sericin possesses antioxidant, antibacterial, and anti-inflammatory properties, making it suitable for skincare and wound healing [5,7,8].

Recent advances in nanotechnology have expanded sericin’s potential by enabling its formulation into nanoparticles, nanofibers, and hydrogels, enhancing its stability and controlled release properties for biomedical and cosmetic applications [9,10]. In wound healing, sericin accelerates tissue repair by promoting fibroblast proliferation and collagen synthesis while reducing inflammation, making it a promising component in advanced wound dressings [1,5,8]. In drug delivery, sericin-based nanocarriers enable controlled and sustained release of therapeutic agents, improving efficacy while reducing side effects [11,12,13].

In cosmetics, sericin contributes to skin hydration, elasticity, and protection against oxidative stress, aligning with the demand for natural, biodegradable ingredients in the cosmeceutical industry [10,14]. Sericin-based formulations have been shown to enhance skin barrier function, reduce trans epidermal water loss, and improve skin smoothness, supporting its integration into premium skincare products. Moreover, sericin’s compatibility with other biopolymers allows it to be blended with hyaluronic acid, collagen, and chitosan for enhanced bioactivity and mechanical properties in both biomedical and cosmetic formulations, expanding its versatility for various applications [12,15].

Despite these promising attributes, challenges remain in scaling sericin extraction with consistent quality and ensuring its stability in complex formulations for nanomaterial development [1,3,16]. Thus, a focused review on sericin-based nanomaterials for biomedical and cosmetic applications is timely to guide further research and practical application [11,17]. This review discusses recent advances, preparation strategies, functional properties, and emerging biomedical and cosmetic uses of sericin-based nanomaterials, providing insights for researchers and industry to harness sericin as a sustainable, high-value biomaterial [18].

Figure 1: Structural morphology of Bombyx mori cocoon, illustrating the transition from the intact cocoon to individual silk fibers enveloped with sericin [19,20,21].

- EXTRACTION, CHARACTERIZATION, AND PROPERTIES OF SERICIN

The extraction of sericin from silk cocoons is a critical step influencing its quality, molecular weight, and functional properties [3,16]. Conventional extraction methods involve hot water, alkaline, acidic, and enzymatic degumming, each impacting the yield and structural integrity of sericin [1,2,5]. A comparative summary of these extraction methods, including their solvents, yields, molecular weight ranges, bioactivity retention, and practical considerations, is presented in Table 1. Hot water extraction preserves bioactivity but may result in lower yields, while alkaline extraction provides higher yield at the cost of partial degradation of sericin chains, affecting its film-forming and moisture-retention properties [7,14,16]. Enzymatic extraction using proteases offers a milder alternative, preserving functional groups while maintaining the biocompatibility necessary for biomedical and cosmetic applications [4,12].

Characterization of sericin involves techniques such as Fourier-transform infrared spectroscopy (FTIR), X-ray diffraction (XRD), differential scanning calorimetry (DSC), and scanning electron microscopy (SEM) to assess structural features, thermal stability, and morphology [9,15]. The amino acid profile, dominated by serine, glycine, and aspartic acid, is responsible for its hydrophilicity and interaction with water molecules, enabling high moisture retention in cosmetic formulations [10,22]. Molecular weight distribution of sericin, typically ranging between 20–400 kDa depending on extraction methods, influences its viscosity, film-forming capacity, and biological activities [6,16].

Sericin’s bioactivity includes antioxidant, antimicrobial, anti-inflammatory, and UV-protective properties, which are critical for wound healing and cosmetic applications [15,18,23]. Its antioxidant capacity helps in scavenging reactive oxygen species, reducing oxidative stress in skin applications, while its antimicrobial activity supports wound healing by preventing infections [1,24]. Additionally, sericin demonstrates excellent film-forming properties, making it suitable for topical applications, providing a protective layer that aids in moisture retention and enhances skin smoothness [14,22].

Recent advancements in nanotechnology have further enhanced sericin’s utility by enabling its formulation into nanoparticles, nanofibers, and hydrogels, which improve its stability, bioavailability, and controlled release in biomedical and cosmetic applications [9,15]. Nanoparticle formulations of sericin have demonstrated improved cellular uptake and targeted delivery of therapeutic agents, while sericin-based hydrogels have shown promise in creating moist environments for wound healing, facilitating faster tissue regeneration [5,8,24]. These properties collectively position sericin as a promising biomaterial for the development of advanced nanomaterial-based applications in the biomedical and cosmetic industries [13,25].

The potential of sericin extends beyond its intrinsic properties, as its compatibility with other natural polymers such as chitosan, collagen, and hyaluronic acid allows for the creation of composite biomaterials with enhanced functionalities [10]. These composites can be engineered to possess specific mechanical properties, biodegradability, and bioactivity tailored to the intended application, whether in skin care, wound management, or drug delivery systems [9,26]. Thus, understanding the extraction methods, structural properties, and functional characteristics of sericin is essential for optimizing its application in nanomaterial development for biomedical and cosmetic uses [15,27].

Table 1: Comparison of Sericin Extraction Methods: Process Parameters and Outcomes

| Methods | Solvent/Conditions | Yield | Molecular weight range | Bioactivity retention | Advantages | Limitations |
| --- | --- | --- | --- | --- | --- | --- |
| Hot water extraction | Boiling water (100oC), 30-36 mins | Moderate | 20–300 kDa | High | Preserves functional groups; eco-friendly | Lower yield; time-consuming |
| Alkaline extraction | Na2CO3, NaOH, pH (9-10), 60-90oC | High | 10–200 kDa | Moderate | Higher yield; faster extraction | Partial degradation of sericin; reduced bioactivity |
| Acidic extraction | Weak acids (citric/acetic acid), 60-90oC | Moderate | 30–250 kDa | Moderate to High | Good bioactivity retention | Corrosive; lower yield than alkaline |
| Enzymatic extraction | Proteases (papain,trypsin), 37-50oC | Low to moderate | 30–400 kDa | Very High | Mild conditions; excellent bioactivity retention | Expensive enzymes; lower yield |
| Novel methods (microwave, ultrasonication, supercritical CO2) | Microwave: 400–600 W, 5–15 min; Ultrasonication: 40 kHz | Moderate to high | Broad (20–400 kDa) | High | Fast; energy-efficient; eco-friendly | Requires specialized equipment |

Note: Data compiled and averaged from multiple studies to provide an indicative comparison of extraction methods, conditions, and outcomes for sericin processing from silk cocoons. For detailed methodologies and results, refer to 1,5,10,15,25,28.

- NANOTECHNOLOGY INTEGRATION: SYNTHESIS AND CHARACTERIZATION OF SERICIN-BASED NANOMATERIALS

The integration of sericin with nanotechnology has revolutionized its application scope, enabling the development of nanoparticles, nanofibers, and hydrogels with enhanced bioavailability, stability, and targeted delivery profiles suitable for advanced biomedical and cosmetic interventions [9,15,29]. This integration has led to the development of diverse sericin-based biomaterials for biomedical and cosmetic applications (Figure 2).

Figure 2: Preparation and biomedical applications of sericin-based biomaterials derived from silk cocoons, highlighting their conversion into hydrogels, nanofibers, films, scaffolds, nanoparticles, and microneedles for therapeutic use [10].

Synthesis techniques such as desolvation, cross-linking, and self-assembly have been employed to fabricate sericin nanoparticles, with the desolvation method using ethanol being particularly effective in producing uniformly sized nanoparticles with controlled morphology [4,10]. Cross-linking with agents such as glutaraldehyde enhances nanoparticle stability, although careful optimization is required to mitigate potential cytotoxicity and maintain biocompatibility [18].

Electrospinning has emerged as a promising approach for producing sericin-based nanofibers due to its capacity to generate high surface area, porous structures that mimic the extracellular matrix, thereby promoting cellular adhesion and proliferation essential for wound healing and tissue engineering applications [5,6,8]. Additionally, the fabrication of sericin-based hydrogels using physical or chemical cross-linking techniques has allowed the development of systems capable of sustained drug release while maintaining a moist environment conducive to accelerated wound healing and skin regeneration [9,13].

Characterization of sericin-based nanomaterials employs a combination of analytical techniques including scanning electron microscopy (SEM), Fourier-transform infrared spectroscopy (FTIR), dynamic light scattering (DLS), and X-ray diffraction (XRD) to confirm morphological integrity, surface properties, particle size distribution, and functional group composition [10,15]. These characterization efforts are pivotal in ensuring that sericin-based nanomaterials meet the physicochemical and biological requirements for their intended biomedical and cosmetic applications while maintaining consistency across production batches [9,27].

- BIOMEDICAL APPLICATIONS OF SERICIN-BASED NANOMATERIALS

  - Wound healing and tissue engineering

Sericin-based nanomaterials have gained recognition as effective wound healing agents due to their antioxidant, antimicrobial, and moisture-retaining properties, collectively supporting a conducive microenvironment for rapid wound closure and tissue regeneration [1,5,8]. Sericin nanoparticles and nanofibers facilitate re-epithelialization, enhance collagen deposition, and promote angiogenesis while reducing inflammation and oxidative stress at wound sites [9,23,24]. The nanostructured architecture of sericin-based dressings enables superior cellular adhesion and migration, which is critical for effective wound closure and healing [11,15].

In tissue engineering, silk-derived natural polymers such as fibroin and sericin have gained significant interest due to their excellent biocompatibility and biodegradability, supporting cell adhesion, migration, proliferation, and differentiation [24,30,31]. Blending sericin with other biopolymers like chitosan and collagen results in composite scaffolds with mechanical stability and bioactivity, suitable for skin grafts, nerve regeneration, and bone tissue engineering [5,6,32]. The biodegradability of sericin ensures gradual resorption, aligning with the tissue regeneration timeline while avoiding adverse immune reactions [8,14,33].

Recent studies have expanded sericin’s role as a scaffold material. For example, Teramoto et al. (2005) developed sericin hydrogels using alcohol without crosslinkers, demonstrating sericin’s promise as a natural biomaterial, while modifications with gelatin and crosslinkers like glutaraldehyde have enhanced sericin’s mechanical properties for use in 2D and 3D scaffold systems [5,14,34]. These scaffolds support fibroblast attachment and proliferation, although higher sericin concentrations may induce cytotoxicity [35]. Nayak et al. (2013) developed 3D porous sericin matrices co-cultured with keratinocytes and fibroblasts for skin tissue engineering, showing successful epidermal and dermal layer formation with low inflammatory responses [36]. Similarly, collagen-sericin scaffolds enriched with hyaluronic acid and chondroitin sulfate have been used for cartilage tissue engineering, supporting adipose-derived stem cell proliferation and differentiation [37].

In stem cell technology, poly(L-lactic-co-ε-caprolactone)-sericin membranes have supported the proliferation and neuronal differentiation of human Wharton’s jelly mesenchymal stem cells, while sericin-based hydrogels combined with collagen and hyaluronic acid have shown promise for dermal applications [30,38,39]. Additionally, thermosensitive chitosan/sericin hydrogels and fibroin/sericin 3D sponges have demonstrated potential in bone tissue engineering, supporting fibroblast attachment, mineralization, and osteogenic differentiation [40,41].

  - Drug Delivery Systems

Sericin’s inherent biocompatibility, biodegradability, and excellent film-forming ability have made it an attractive material for advanced drug delivery systems in modern biomedical applications [26]. Its molecular structure allows the encapsulation of diverse therapeutic agents, including antibiotics, anti-inflammatory drugs, anticancer drugs, and growth factors, protecting them from premature degradation while facilitating their controlled and sustained release at the target site [9,13].

Nanoparticle formulations of sericin can be tailored to achieve specific release kinetics by adjusting parameters such as particle size, cross-linking density, and surface modification [12,15]. These controlled-release systems can reduce dosing frequency, enhance therapeutic efficacy, and minimize systemic side effects, thereby improving patient compliance. Moreover, sericin’s hydrophilicity supports its integration with hydrophobic drugs, enabling enhanced solubility and bioavailability in physiological environments [14,26].

The integration of sericin into transdermal drug delivery systems has opened new avenues for non-invasive therapy, particularly for managing chronic diseases and localized treatment of skin conditions [4,10]. In these systems, sericin not only acts as a carrier but also contributes to skin hydration and barrier function, facilitating enhanced permeation of drugs across the stratum corneum while maintaining skin health. Studies have demonstrated the potential of sericin-based hydrogels and nanofibers to deliver bioactive molecules efficiently while providing a moist environment conducive to healing [9,14].

Additionally, sericin has shown promise in the oral delivery of bio-actives, where it can protect sensitive therapeutic molecules from the harsh gastric environment, enabling targeted release in the intestines. This versatility positions sericin as a valuable material in the development of next-generation drug delivery platforms that are sustainable, effective, and patient-friendly [42].

  - Antioxidant and Anti-inflammatory Applications

Oxidative stress and inflammation are key contributors to various chronic diseases, including diabetes, cardiovascular disorders, and skin aging. Sericin’s potent antioxidant and anti-inflammatory properties have been extensively explored for their therapeutic applications in combating oxidative damage and modulating inflammatory responses [1,5].

Sericin possesses amino acids such as serine and threonine, which contribute to its reactive oxygen species (ROS) scavenging activity, thereby protecting cellular components from oxidative damage and supporting cellular homeostasis [14,18]. Kato et al. (1998) first demonstrated sericin’s capability to inhibit lipid peroxidation, a significant factor in the progression of diseases like hypertension and diabetes [43,44]. Furthermore, sericin’s anti-tyrosinase activity is crucial in controlling melanin biosynthesis, making it relevant in both cosmetic skin-lightening formulations and food preservation [45].

Additionally, sericin modulates inflammatory cytokines such as TNF-α, IFN-γ, and IL-10, which are pivotal in inflammatory pathways, suggesting its role in managing conditions characterized by chronic inflammation [15]. These properties make sericin a multifunctional bioactive suitable for therapeutic formulations aimed at reducing oxidative stress, managing inflammation-driven diseases, and supporting tissue regeneration while offering protective benefits in cosmeceutical products [10,12].

  - Antimicrobial Applications

Sericin exhibits inherent antimicrobial activity against various bacterial strains, including Staphylococcus aureus and Escherichia coli, making it a potential bioactive agent in preventing infections in wound dressings and implants [7,46]. This property is particularly valuable in the context of rising antimicrobial resistance, where there is a critical need for safe, natural alternatives to synthetic antimicrobials in healthcare settings [28].

The antimicrobial action of sericin is primarily attributed to its ability to disrupt bacterial cell membranes and interfere with cellular metabolism, leading to effective bacterial inhibition while maintaining non-toxicity toward human cells [1]. When sericin is incorporated into nanostructured systems such as nanoparticles, nanofibers, and hydrogels, its surface contact with microbial cells increases, further enhancing its antimicrobial efficacy in biomedical applications [5,13,25,27].

In wound healing, sericin-based nanomaterials serve a dual role by supporting rapid tissue regeneration while simultaneously preventing infection at the wound site. This reduces the need for systemic antibiotic administration, thereby contributing to strategies aimed at combating antimicrobial resistance while promoting faster and safer wound healing [46,47]. Additionally, sericin’s compatibility with other antimicrobial agents allows for the development of synergistic composite materials, expanding its applicability in advanced wound dressings, implant coatings, and biomedical devices requiring infection prevention and bioactivity. These properties collectively position sericin as a promising, sustainable material for next-generation antimicrobial biomedical applications [12,28,46].

  - Bone Regeneration

Emerging research highlights sericin’s potential in bone tissue engineering due to its capacity to promote osteoblast adhesion, proliferation, and extracellular matrix formation when incorporated into composite scaffolds with hydroxyapatite or bioglass [6,15]. Sericin enhances mineralization and supports the deposition of calcium phosphate within scaffolds, facilitating effective bone regeneration while providing a biodegradable and biocompatible environment essential for orthopaedic and dental applications [5,32,33].

Its amino acid composition aids in calcium ion chelation, stimulating hydroxyapatite crystallization and scaffold osteoconductivity [1,32]. Additionally, sericin-based composites can modulate osteogenic signalling pathways, promoting stem cell differentiation into osteogenic lineages, which is critical for bone tissue repair while ensuring biocompatibility and gradual biodegradation aligned with new tissue formation [18,31].

Studies demonstrate that the incorporation of sericin into composite scaffolds improves mechanical properties, porosity, and bioactivity, enhancing the scaffold’s ability to support cell infiltration, nutrient diffusion, and vascularization, all of which are essential for successful bone regeneration [5,6]. Additionally, sericin’s inherent antioxidant and antimicrobial properties further contribute to creating a favourable microenvironment for bone healing, reducing oxidative stress and infection risks at the implantation site [24,28].

These collective attributes position sericin-based nanomaterials and composite scaffolds as promising candidates for the development of next-generation bone tissue engineering strategies, addressing current limitations in bone grafting and synthetic biomaterials while aligning with the goals of biocompatibility, biodegradability, and enhanced functional recovery in orthopaedic and dental applications [10,48].

  - Sericin in Culture Media and Cryopreservation

Cryopreservation and cell culture are essential components of regenerative medicine, biobanking, and advanced cellular therapies. Traditionally, fetal bovine serum (FBS) has been used as a supplement in cell culture media; however, it poses risks of contamination and immunogenic reactions [49]. Sericin has emerged as a safe, effective alternative to FBS, demonstrating the ability to support cell proliferation, maintain cell viability, and enhance the quality of preserved cells across various cell types. Sericin with varying molecular weights has been shown to stimulate the proliferation of hybridoma cells, with lower molecular weight sericin (5–100 kDa) being particularly effective [50]. It has been successfully applied in culturing human dermal fibroblasts, keratinocytes, PC12 rat pheochromocytoma cells, and Sf9 insect cells in serum-free media, maintaining robust proliferation while reducing contamination risks [49].

In cryopreservation, sericin supplementation improves antioxidant stability in freezing media, maintaining membrane integrity and motility in preserved sperm cells, as demonstrated in studies with buffalo sperm [51]. It has also been used in culturing rat islet cells and insulinoma cell lines [52]. Terada et al. (2005) showed that low concentrations of sericin (0.01–0.1%) effectively support hybridoma cell proliferation, while Verdanova et al. (2014) reported that 1% sericin in 10% DMSO provided effective cryoprotection for human mesenchymal stromal cells (hMSCs) [50,53]. Overall, sericin’s ability to replace foetal bovine serum (FBS) in culture media while enhancing cell viability and proliferation during cryopreservation underscores its role as a sustainable, biocompatible solution in cellular engineering, regenerative medicine, and biobanking applications [54,55].

- COSMETIC APPLICATIONS OF SERICIN-BASED NANOMATERIALS

  - Moisturization and Skin Barrier Enhancement

Sericin has emerged as a valuable component in cosmetic formulations due to its excellent moisturizing, antioxidant, and film-forming properties [17]. It forms a thin protective film on the skin, reducing transepidermal water loss and enhancing moisture retention, thereby improving skin elasticity and smoothness [10,14]. The high content of hydrophilic amino acids, including serine and aspartic acid, facilitates deep hydration, making sericin ideal for moisturizers and anti-aging products [1,22].

Sericin’s excellent biocompatibility, biodegradability, and wettability have led to its use in a variety of cosmetic products for skin, hair, and nails, either on its own or combined with silk fibroin. When included in lotions, creams, and ointments, sericin has been shown to enhance skin elasticity while providing anti-wrinkle and anti-aging benefits [1, 56]. It is a key ingredient in moisturizers formulated to combat skin dryness by maintaining hydration in the outermost skin layers [13,17,22]. Moisturizers often include wetting agents such as vegetable glycerine, water, jojoba oil, vitamin E oil, and sorbitol, enhancing the hydrating capabilities of sericin-based formulations [57].

Sericin gels containing hydroxyproline have been found to increase epidermal thickness and reduce skin impedance, reflecting its superior moisturizing capacity [22,58]. In vivo studies have confirmed that sericin increases hydroxyproline levels, hydrates epidermal cells, and reduces skin impedance, with the proline content aiding collagen production while limiting transepidermal water loss to prevent dryness [22,56]. By retaining moisture within the stratum corneum, sericin helps keep the skin smooth and plump, making it a highly effective component in moisturizing skincare formulations [17,58].

In skin conditions like atopic dermatitis and ichthyosis, which reduce free amino acids in the stratum corneum and cause dryness, sericin has shown therapeutic promise. Kim et al. (2012) demonstrated that a 1% sericin application effectively alleviates skin dryness in atopic dermatitis, while dietary sericin intake enhances hydration by increasing filaggrin and free amino acids in the stratum corneum, inducing gene expressions critical for skin barrier function, such as PPARγ, PAD3, and caspase-14, thus establishing its role in dry skin management [9,59].

Sericin is highly hygroscopic and inhibits melanin synthesis in the skin’s cortical layers, making it valuable for skin-brightening cosmetic applications. The molecular weight of sericin influences its application: 12,000–17,000 Da for haircare and 5,000–70,000 Da for skin-care products [17,58,60]. Its amino acid composition closely resembles the natural moisturizing factors in the stratum corneum, which maintain skin hydration [13,58,59]. Combining 1% sericin with 4% D-glucose in lotions provides effective hydration and conditioning benefits [17,56]. Sericin-based creams exhibit enhanced cleansing with reduced skin irritation [17,61] while its addition to sunscreen formulations boosts the light-screening effects of UV filters like triazines and cinnamic acid esters [17].

Additionally, sericin helps absorb sweat and sebum, contributing to cleaner, healthier skin [17]. Sericin’s antioxidant activity neutralizes reactive oxygen species, reducing oxidative stress and preventing premature aging due to UV radiation and pollution [5]. It also supports collagen synthesis while inhibiting matrix metalloproteinases, enhancing skin firmness and reducing fine lines and wrinkles [15]. Furthermore, its film-forming ability reinforces the skin barrier against pollutants while maintaining hydration, making it highly suitable for sensitive and dry skin formulations [10].

  - Anti-Aging and Skin Rejuvenation

Sericin has shown remarkable potential in anti-aging formulations due to its fibroblast-stimulating and collagen synthesis-enhancing properties, which help maintain skin elasticity and structure, reducing the visibility of fine lines and wrinkles [6,10]. By inhibiting collagenase activity, sericin preserves existing collagen networks while promoting the formation of new collagen fibers, critical for maintaining skin firmness and resilience [5,15]. Additionally, sericin’s antioxidant capabilities counteract reactive oxygen species generated by UV exposure and environmental pollutants, thereby reducing oxidative stress-induced skin aging and photoaging effects [9,14].

Studies indicate that sericin, when incorporated into creams and serums, can improve skin texture, hydration, and radiance, making it a valuable ingredient in advanced skincare regimes [10,17]. Its compatibility with other anti-aging agents like hyaluronic acid and vitamin E further enhances sericin’s ability to support skin rejuvenation while maintaining moisture and barrier function, aligning with the demand for multifunctional cosmeceutical products [5,13]. This multifaceted approach positions sericin as a sustainable, bioactive component for next-generation anti-aging skincare formulations.

  - Skin Brightening and Anti-Hyperpigmentation

Sericin demonstrates anti-tyrosinase activity, which helps regulate melanin synthesis, providing an effective and natural approach to managing hyperpigmentation and promoting a brighter, more even skin tone [4,15]. By inhibiting excessive melanin production, sericin-based skincare formulations address conditions such as melasma, age spots, and post-inflammatory hyperpigmentation without the harsh side effects often associated with synthetic brightening agents [5,10]. Moreover, sericin’s antioxidant properties further contribute to skin brightening by neutralizing oxidative stress that can trigger pigmentation pathways, thereby reduce the recurrence of dark spots and promote skin clarity [14,46].

Recent studies have shown that combining sericin with vitamin C, niacinamide, or botanical extracts enhances the skin-brightening effect synergistically while providing hydration and anti-inflammatory benefits, supporting comprehensive skin tone improvement [5,15]. The biocompatibility and mild nature of sericin make it ideal for sensitive skin types, providing effective brightening without irritation, which is crucial in consumer-friendly brightening formulations [9,17].

  - Sericin-Based Nanocarriers for Active Ingredient Delivery

The application of sericin as a nanocarrier system represents a significant advancement in cosmeceuticals, enhancing the delivery and stability of active ingredients such as vitamins, peptides, botanical antioxidants, and coenzymes used in skincare [5,15,17,46]. Sericin-based nanoparticles and nanofibers encapsulate these actives, protecting them from environmental degradation and enzymatic breakdown while ensuring controlled and targeted delivery into deeper skin layers [9,13].

This targeted delivery enhances the bioavailability and efficacy of actives, allowing lower concentrations to achieve desired effects while reducing potential irritation [10,14]. For example, sericin-based nanocarriers delivering vitamin C can improve collagen synthesis and brightening effects while maintaining stability, which is often a challenge in conventional formulations [10,11].

Additionally, sericin’s inherent film-forming and hydrophilic properties aid in prolonged skin contact and moisture retention, further boosting the functionality of active ingredients delivered through these nanocarriers [5,10]. As consumer demand grows for high-performance, targeted, and sustainable skincare, sericin-based nanocarriers align well with industry trends, supporting the development of innovative, clean-label cosmetic products [17,46].

  - Scalp and Hair Care Applications

In hair care, sericin’s moisture-retaining and film-forming abilities make it valuable for improving hair hydration, reducing frizz, and enhancing shine and smoothness in shampoos, conditioners, and hair masks [1,15,17]. By forming a protective layer around the hair shaft, sericin reduces hair breakage and split ends caused by mechanical stress and environmental damage while preserving hair structure [5,6]. Sericin’s antioxidant properties also contribute to scalp health by reducing oxidative stress, which can impact hair follicle vitality and contribute to hair thinning and loss [10,14].

Incorporating sericin into scalp treatments and serums can help maintain scalp hydration and protect against UV and pollution-induced damage, promoting a healthier scalp environment conducive to hair growth [58,62]. Additionally, sericin’s biodegradability and compatibility with botanical extracts and vitamins enhance the performance of hair care formulations, making them suitable for sensitive scalps and environmentally conscious consumers [10,15]. These properties collectively position sericin as a multifunctional, sustainable ingredient for next-generation hair and scalp care innovations.

- MECHANISMS UNDERPINNING BIOMEDICAL AND COSMETIC EFFICACY

The multifunctionality of sericin in biomedical and cosmetic applications is primarily driven by its amino acid composition, molecular structure, and bioactivity [27]. The high content of hydrophilic amino acids facilitates moisture retention, which is crucial for maintaining skin hydration and creating a moist environment for wound healing, promoting cell proliferation and tissue regeneration [1,6]. Sericin’s antioxidant properties, derived from its ability to scavenge reactive oxygen species, play a pivotal role in reducing oxidative stress, thereby protecting skin from environmental damage and accelerating wound healing [5,15,24].

Biodegradability is another essential property, ensuring that sericin and its nanostructures degrade into non-toxic byproducts within the body, minimizing adverse immune responses and supporting safe biomedical use [9,14]. The integration of sericin into nanomaterials further enhances its stability and facilitates targeted delivery, improving its therapeutic outcomes in drug delivery and skincare formulations [10,23]. These mechanisms collectively position sericin-based nanomaterials as effective and versatile tools in the development of sustainable healthcare and cosmetic products [12].

- CHALLENGES AND FUTURE PROSPECTS

Despite its promising potential, the widespread application of sericin-based nanomaterials faces several challenges that require systematic attention. Variability in extraction methods leads to differences in molecular weight and bioactivity of sericin, necessitating standardization to ensure consistency in product performance across batches [4,15,16]. Stability issues during storage, including nanoparticle aggregation and degradation, require the development of effective stabilization strategies to maintain the functional properties of sericin-based formulations [10,13].

Regulatory hurdles remain a significant challenge, particularly for clinical applications of sericin-based biomedical products, necessitating comprehensive toxicological and efficacy studies to secure approvals [9,46]. In the cosmetic industry, regulatory compliance with safety standards is essential to ensure consumer acceptance and trust in sericin-based skincare formulations [5,15].

Future directions should focus on optimizing extraction and purification processes for scalable production, exploring novel composite materials integrating sericin with other biopolymers, and developing stimuli-responsive nanocarriers for precision therapy and targeted skincare applications [6,14]. Advanced techniques such as 3D bioprinting, bioelectronics integration, and functionalization of sericin with therapeutic molecules hold promise for expanding the application landscape of sericin-based nanomaterials, positioning them as next-generation sustainable solutions in healthcare and cosmetic industries [5,9].

- CONCLUSION

Sericin has transitioned from being a discarded by-product of the silk industry to a high-value biomaterial with broad applications in the biomedical and cosmetic sectors. Its inherent biocompatibility, biodegradability, antioxidant, and moisture-retention properties align well with the demands of modern healthcare and skincare products aimed at promoting wellness while maintaining environmental sustainability. The integration of sericin with nanotechnology has further amplified its utility, facilitating the development of innovative wound dressings, drug delivery systems, and advanced skincare formulations with enhanced efficacy and stability. Addressing current challenges related to standardization, stability, and regulatory compliance will be essential to translating laboratory advancements into commercially viable products. Continued interdisciplinary research focusing on the functionalization and application of sericin-based nanomaterials will contribute significantly to developing sustainable, effective, and consumer-friendly healthcare and cosmetic products, firmly positioning sericin as a critical biomaterial in the advancement of next-generation bio-based industries.

References

- Padamwar MN, Pawar AP. Silk sericin and its applications: A review. Journal of Scientific and Industrial Research. 2004; 63, 323–329.

- Capar G, Pilevneli T, Yetis U, Dilek FB. Life cycle assessment of sericin recovery from silk degumming wastewaters. Sustainable Chemistry and Pharmacy. 2022; 30, 100889.

- Sabu Mathew S, Maria HJ, Allardyce BJ, Rajkhowa R, Thomas S. Waste to wealth: exploring the versatile prospects of discarded silk sericin. ACS Sustainable Chemistry & Engineering. 2024; 12(3), 1165-1184.

- Zhaorigetu S, Yanaka N, Sasaki M, Watanabe H, Kato N. Inhibitory effects of silk protein, sericin on UVB-induced acute damage and tumor promotion by reducing oxidative stress in the skin of hairless mouse. Journal of Photochemistry and Photobiology B: Biology. 2003; 71(1-3), 11-17.

- Lamboni L, Gauthier M, Yang G, Wang Q. Silk sericin: A versatile material for tissue engineering and drug delivery. Biotechnology advances. 2015; 33(8), 1855-1867.

- Vepari C, Kaplan DL. Silk as a biomaterial. Progress in polymer science. 2007; 32(8-9), 991-1007.

- Kurioka A, Yamazaki M. Antioxidant in the cocoon of the silkworm, Bombyx mori. Journal of Insect Biotechnology and Sericology. 2002; 71(3), 177-180.

- Mazurek Ł, Rybka M, Jurak J, Frankowski J, Konop M. Silk sericin and its effect on skin wound healing: A state of the art. Macromolecular Bioscience. 2024; 24(10), 2400145.

- Stradczuk‐Mazurek M, Mazurek Ł, Konop M. Silk Sericin in Dermatological Diseases: From Preclinical Studies to Future Clinical Applications. Macromolecular Bioscience. 2025; e00058.

- Ma Q, Salathia S, Gigliobianco MR, Casadidio C, Di Martino P, Censi R. Recent Insights into the Potential and Challenges of Sericin as a Drug Delivery Platform for Multiple Biomedical Applications. Pharmaceutics. 2025; 17(6), 695.

- Liu J, Shi L, Deng Y, Zou M, Cai B, Song Y, Wang Z, Wang L. Silk sericin-based materials for biomedical applications. Biomaterials. 2022; 287, 121638.

- Silva AS, Costa EC, Reis S, Spencer C, Calhelha RC, Miguel SP, Ribeiro MP, Barros L, Vaz JA, Coutinho P. Silk sericin: a promising sustainable biomaterial for biomedical and pharmaceutical applications. Polymers. 2022; 14(22), 4931.

- Aad R, Dragojlov I, Vesentini S. Sericin protein: structure, properties, and applications. Journal of Functional Biomaterials. 2024; 15(11), 322.

- Mandal BB, Priya AS, Kundu SC. Novel silk sericin/gelatin 3-D scaffolds and 2-D films: fabrication and characterization for potential tissue engineering applications. Acta Biomaterialia. 2009; 5(8), 3007-3020.

- Suryawanshi, R., Kanoujia, J., Parashar, P., & Saraf, S. (2020). Sericin: A versatile protein biopolymer with therapeutic significance. Current Pharmaceutical Design, 26(42), 5414-5429.

- Vaishnav SR, Singh SA. Sericin, a by-product of the silk industry: Extraction and applications. In Value-Addition in Agri-Food Industry Waste Through Enzyme Technology. 2023; (pp. 199-208). Academic Press.

- Joseph PS, Selvasudha N, Unnikrishnan Meenakshi D, Ganesan P, Thekkila‐Veedu S, Pathayappurakkal Mohanan D, George AM, Kandasamy R. Pharmaceutical, Therapeutic, and Cosmetic Applications of Sericin. Biopolymers in Pharmaceutical and Food Applications. 2024; 2, 641-670.

- Aramwit P, Siritientong T, Kanokpanont S, Srichana T. Formulation and characterization of silk sericin–PVA scaffold crosslinked with genipin. International journal of biological macromolecules. 2010a; 47(5), 668-675.

- Chen F, Porter D, Vollrath F. Structure and physical properties of silkworm cocoons. Journal of the Royal Society Interface. 2012; 9(74), 2299-2308.

- Cao TT, Zhang YQ. Processing and characterization of silk sericin from Bombyx mori and its application in biomaterials and biomedicines. Materials Science and Engineering: C. 2016; 61, 940-952.

- Reis S, Spencer C, Soares CM, Falcão SI, Miguel SP, Ribeiro MP, Barros L, Coutinho P, Vaz J. Chemical characterization and bioactivities of sericin extracted from silkworm cocoons from two regions of Portugal. Molecules. 2025; 30(5), 1179.

- Padamwar MN, Pawar AP, Daithankar AV, Mahadik KR. Silk sericin as a moisturizer: an in vivo study. Journal of Cosmetic Dermatology. 2005; 4(4), 250-257.

- Aramwit P, Kanokpanont S, Nakpheng T, Srichana T. The effect of sericin from various extraction methods on cell viability and collagen production. International Journal of Molecular Sciences. 2010b; 11(5), 2200-2211.

- Veiga A, Foster O, Kaplan DL, Oliveira AL. Expanding the boundaries of silk sericin biomaterials in biomedical applications. Journal of Materials Chemistry B. 2024; 12(29), 7020-7040.

- Wang J, Liu H, Shi X, Qin S, Liu J, Lv Q, Liu J, Li Q, Wang Z, Wang, L. Development and application of an advanced biomedical material‐silk sericin. Advanced Materials. 2024a; 36(23), 2311593.

- Kumar SSD, Abrahamse H. Sericin-based nanomaterials and their applications in drug delivery. In Bio-Based Nanomaterials. 2022; (pp. 211-229). Elsevier.

- Holland C, Numata K, Rnjak‐Kovacina J, Seib FP. The biomedical use of silk: past, present, future. Advanced healthcare materials. 2019; 8(1), 1800465.

- Wang SL, Zhuo JJ, Fang SM, Xu W, Yu QY. Silk sericin and its composite materials with antibacterial properties to enhance wound healing: a review. Biomolecules. 2024b; 14(6), 723.

- Mondal M, Trivedy K, Nirmal KS. The silk proteins, sericin and fibroin in silkworm, Bombyx mori Linn.,- a review. 2007.

- Wang F, Wang Y, Tian C, Xu S, Wang R, Hou K, Chen W, Zhao P, Lu Z, Kaplan DL, Xia Q. Fabrication of the FGF1-functionalized sericin hydrogels with cell proliferation activity for biomedical application using genetically engineered Bombyx mori (B. mori) silk. Acta biomaterialia. 2018; 79, 239-252.

- Li G, Sun S. Silk fibroin-based biomaterials for tissue engineering applications. Molecules. 2022; 27(9), 2757.

- Ding Z, Cheng W, Mia MS, Lu Q. Silk biomaterials for bone tissue engineering. Macromolecular bioscience. 2021; 21(8), 2100153.

- Zhu J, Du Y, Backman LJ, Chen J, Ouyang H, Zhang W. Cellular interactions and biological effects of silk fibroin: implications for tissue engineering and regenerative medicine. Small. 2025; 21(4), 2409739.

- Teramoto H, Nakajima KI, Takabayashi C. Preparation of elastic silk sericin hydrogel. Bioscience, biotechnology, and biochemistry. 2005; 69(4), 845-847.

- Nayak S, Talukdar S, Kundu SC. Potential of 2D crosslinked sericin membranes with improved biostability for skin tissue engineering. Cell and tissue research. 2012; 347(3), 783-794.

- Nayak S, Dey S, Kundu SC. Skin equivalent tissue-engineered construct: co-cultured fibroblasts/keratinocytes on 3D matrices of sericin hope cocoons. PloS one. 2013; 8(9), e74779.

- Dinescu S, Gălăţeanu B, Albu M, Lungu A, Radu E, Hermenean A, Costache M. Biocompatibility Assessment of Novel Collagen‐Sericin Scaffolds Improved with Hyaluronic Acid and Chondroitin Sulfate for Cartilage Regeneration. BioMed research international. 2013; 2013(1), 598056.

- Inthanon K, Daranarong D, Techaikool P, Punyodom W, Khaniyao V, Bernstein AM, Wongkham W. Biocompatibility Assessment of PLCL‐Sericin Copolymer Membranes Using Wharton’s Jelly Mesenchymal Stem Cells. Stem Cells International. 2016; 2016(1), 5309484.

- Vulpe R, Popa M, Picton L, Peptu CA, Tudorachi N, Verestiuc L. Scaffolds based on collagen, hyaluronan and sericin with potential applications as controlled drug delivery system. Journal of Nanoscience and Nanotechnology. 2018; 18(3), 1528-1533.

- Pankongadisak P, Suwantong O. The potential use of thermosensitive chitosan/silk sericin hydrogels loaded with longan seed extract for bone tissue engineering. RSC advances. 2018; 8(70), 40219-40231.

- Siavashani AZ, Mohammadi J, Rottmar M, Senturk B, Nourmohammadi J, Sadeghi B, Huber L, Maniura-Weber K. Silk fibroin/sericin 3D sponges: The effect of sericin on structural and biological properties of fibroin. International journal of biological macromolecules. 2020; 153, 317-326.

- Ma Y, Tong X, Huang Y, Zhou X, Yang C, Chen J, Dai F, Xiao, B. Oral administration of hydrogel-embedding silk sericin alleviates ulcerative colitis through wound healing, anti-inflammation, and anti-oxidation. ACS Biomaterials Science & Engineering. 2019; 5(11), 6231-6242.

- Kato N, Sato S, Yamanaka A, Yamada H, Fuwa N, Nomura M. Silk protein, sericin, inhibits lipid peroxidation and tyrosinase activity. Bioscience, biotechnology, and biochemistry. 1998; 62(1), 145-147.

- Walter MF, Jacob RF, Jeffers B, Ghadanfar MM, Preston GM, Buch J, Mason RP. Serum levels of thiobarbituric acid reactive substances predict cardiovascular events in patients with stable coronary artery disease: a longitudinal analysis of the PREVENT study. Journal of the American College of Cardiology. 2004; 44(10), 1996-2002.

- Cavalieri EL, Li KM, Balu N, Saeed M, Devanesan P, Higginbotham S, Zhao J, Gross ML, Rogan EG. Catechol ortho-quinones: the electrophilic compounds that form depurinating DNA adducts and could initiate cancer and other diseases. Carcinogenesis. 2002; 23(6), 1071-1077.

- Das G, Shin HS, Campos EVR, Fraceto LF, del Pilar Rodriguez-Torres M, Mariano KCF, Ribeiro de Araujo D, Fernández-Luqueño F, Grillo R, Patra JK. Sericin based nanoformulations: a comprehensive review on molecular mechanisms of interaction with organisms to biological applications. Journal of Nanobiotechnology. 2021; 19(1), 30.

- Munir F, Tahir HM, Ali S, Ali A, Tehreem A, Zaidi SDES, Adnan M, Ijaz F. Characterization and evaluation of silk sericin-based hydrogel: a promising biomaterial for efficient healing of acute wounds. ACS omega. 2023; 8(35), 32090-32098.

- Waidi YO, Debnath S, Datta S, Chatterjee K. 3D-Printed silk proteins for bone tissue regeneration and associated immunomodulation. Biomacromolecules. 2024; 25(9), 5512-5540.

- Sasaki M, Kato Y, Yamada H, Terada S. Development of a novel serum‐free freezing medium for mammalian cells using the silk protein sericin. Biotechnology and applied biochemistry. 2005; 42(2), 183-188.

- Terada S, Sasaki M, Yanagihara K, Yamada H. Preparation of silk protein sericin as mitogenic factor for better mammalian cell culture. Journal of Bioscience and Bioengineering. 2005; 100(6), 667-671.

- Vijyeta HP, Kavani FS, Vagh AA, Solanki GB, Vala KB, Singh VK, Dham AJ. Effect of supplementation of antioxidant sericin in semen extender on post-thaw sperm quality, oxidative status, and fertility of Jaffarabadi buffalo bull semen. Indian J. Vet. Sci. Biotechnol. 2024; 20(2), 79-84.

- Ogawa A, Terada S, Saito Y, Kimura T, Yamaguchi A, Miki M. CrmA and Bcl-2 protect a cell line derived from islet of Langerhans, RIN-5F from hypoxia-induced apoptosis. Biochemical engineering journal. 2004; 20(2-3), 209-215.

- Verdanova M, Pytlik R, Kalbacova MH. Evaluation of sericin as a fetal bovine serum-replacing cryoprotectant during freezing of human mesenchymal stromal cells and human osteoblast-like cells. Biopreservation and biobanking. 2014; 12(2), 99-105.

- Cao TT, Zhang YQ. Viability and proliferation of L929, tumour and hybridoma cells in the culture media containing sericin protein as a supplement or serum substitute. Applied microbiology and biotechnology. 2015; 99(17), 7219-7228.

- Cao TT, Zhang YQ. The potential of silk sericin protein as a serum substitute or an additive in cell culture and cryopreservation. Amino Acids. 2017; 49(6), 1029-1039.

- Mendoza‐Muñoz N, Leyva‐Gómez G, Piñón‐Segundo E, Zambrano‐Zaragoza ML, Quintanar‐Guerrero D, Del Prado Audelo ML, Urbán‐Morlán Z. Trends in biopolymer science applied to cosmetics. International Journal of Cosmetic Science. 2023; 45(6), 699-724.

- Kirikawa M, Kasaharu T, Kishida K, Akiyama D. Silk protein micropowders for coating with excellent feeling, antistaticity and moisture absorbability and releasability and their manufacture. In Chemical Abstracts. 2000; (Vol. 132, No. 1, p. 8).

- Hari AS, Kandasubramanian B. Silk Biopolymer in Cosmetics: Efficacy, Utilization and Commercial Perspectives. In Engineering Natural Silk: Applications and Future Directions. 2024; (pp. 155-176). Singapore: Springer Nature Singapore.

- Kim H, Lim YJ, Park JH, Cho Y. Dietary silk protein, sericin, improves epidermal hydration with increased levels of filaggrins and free amino acids in NC/Nga mice. British Journal of Nutrition. 2012; 108(10), 1726-1735.

- Sheng J Y, Xu J, Zhuang Y, Sun DQ, Xing TL, Chen GQ. Study on the application of sericin in cosmetics. Advanced materials research. 2013; 796, 416-423.

- Takechi T, Wada R, Fukuda T, Harada K, Takamura H. Antioxidant activities of two sericin proteins extracted from cocoon of silkworm (Bombyx mori) measured by DPPH, chemiluminescence, ORAC and ESR methods. Biomedical reports. 2014; 2(3), 364-369.

- Ristić N, Nikolić DM, Zdravković A, Mičić A, Ristić I. Biofunctional textile materials: cosmetic textiles. Advanced Technologies. 2022; 11(1), 63-75.