| Journal Name: | Journal of Materials Science Research and Reviews |
| --- | --- |
| Manuscript Number: | Ms_JMSRR_142005 |
| Title of the Manuscript: | Hemp as Bio Fiber Material for Paper Applications – Fiber Processing |
| Type of the Article | Original Research Article |

| ## PART 1: Comments |  |  |
| --- | --- | --- |
|  | ## Reviewer’s comment Artificial Intelligence (AI) generated or assisted review comments are strictly prohibited during peer review. | Author’s Feedback (It is mandatory that authors should write his/her feedback here) |
| Please write a few sentences regarding the importance of this manuscript for the scientific community. A minimum of 3-4 sentences may be required for this part. | Using hemp as a bio fiber for paper applications, because hemp paper is recyclable, compostable, and biodegradable, it promotes the objectives of the circular economy. Demand for sustainable fibers is rising as a result of governments and businesses promoting carbon neutrality. In this manuscript hand sheets were prepared according to TAPPI test method T 205 sp-12, Forming hand sheets for physical tests of pulp. Physical testing of hand sheets was performed in accordance with TAPPI test method T 220 sp-06, Physical testing of pulp hand sheets. Refining the hemp fibers at 60°C in a KRK pressured refiner is the most promising phase. It is advised to cut the hemp stems into 0.75-inch (19.0 mm) lengths before refining and to run the refiner plates at 1800 rpm with a 0.5 mm gap. It is advised that all refined hemp fibers be screened using a Valley type screen with a 150 µm screen plate and a screen box with a 150 mesh (105 µm) sieve fabric to collect the processed fiber material. The final CSF is then adjusted using a Valley beater type machine to produce the desired fiber material for hand sheet making. This will lessen the tendency of the hemp fibers to string. |  |
| Is the title of the article suitable? (If not please suggest an alternative title) | Yes, title is absolutely suitable. |  |
| ## Is the abstract of the article comprehensive? Do you suggest the addition (or deletion) of some points in this section? Please write your suggestions here. | Abstract should be refined and length will be crispy. |  |
| ## Is the manuscript scientifically, correct? Please write here. | The manuscript is almost scientific, indeed. To demonstrate the innovation of the current work, the author should discuss the accomplishments and shortcomings of the earlier work. |  |
| Are the references sufficient and recent? If you have suggestions of additional references, please mention them in the review form. | Yes, there is satisfactory references were provided in this paper. |  |
| ## Is the language/English quality of the article suitable for scholarly communications? | Quality of the English should be improved. I sincerely advise the authors to rephrase a couple of sentences throughout the manuscript. |  |
| ## Optional/General comments |  |  |

| PART 2: |  |  |
| --- | --- | --- |
|  | - Reviewer’s comment | - Author’s comment (if agreed with reviewer, correct the manuscript and highlight that part in the manuscript. It is mandatory that authors should write his/her feedback here) |
| Are there ethical issues in this manuscript? | (If yes, Kindly please write down the ethical issues here in details) |  |

Reviewer details:

I.S.N.V.R. Prasanth, Malla Reddy Engineering College, India