Synthesis and crystal structure of poly[bis(1-ethyl-2,5-dihydro-1H-imidazole-κN3)(succinato-κO)copper(II)]

______________________________________________________________________

ABSTRACT

The new title copper(II) succinato complex [Cu(O2C(CH2)2CO2)(C3H5N2C2H5)2]n (1) has been isolated as single crystals state from one pot reaction between HO2C(CH2)2CO2H (succinic acid), C3H5N2C2H5 (1-ethyl-2,5-dihydro-1H-imidazole) and Cu(CH3COO)2 in distilled water. Compound 1 has been characterized by elemental analysis, FTIR spectroscopy and X-ray diffraction. In the solid state, 1 crystallizes in the orthorhombic chiral system P212121 space group with a = 9.8406(3) Å, b = 12.6318(3) Å, c = 13.0246(4) Å,  =  =  = 90°, V = 1619.016 Å3 and Z = 4. The asymmetric unit of the copper(II) complex is formed by one central copper(II), two imidazole molecules and one succinate unit. The copper(II) ion is tetra-coordinated by two nitrogen atoms from imidazole molecules acting in η1-mode, one oxygen atom from succinate anion and one oxygen atom from succinate anion of a neighboring molecule complex. In the structure the copper(II) cation is situated in N2O2 inner, and its environment is best described as square planar geometry. Each arm of the succinate anions acts in η1-mode, and the succinate units act as bridge between two copper(II) centers developing a polymer coordination. In the crystal, unclassical hydrogen bonds of type C—H···O involving the coordinated and the non-coordinated oxygen atoms of the succinate groups as donor atoms, generate a supramolecular network. The overall structure consists of parallel infinite chains of Cu(C4O4H4)(C3H5N2C2H5)2, each parallel chain extending along the b axis.

Keywords: Succinic acid, imidazole, copper(II), complex, infrared, crystal, X-ray

# INTRODUCTION

Succinic acid is a widely used compound in industry. It is used as an acidulant in the food industry and as a precursor in the production of polyester and resins. Extensive studies have shown it to be non-toxic. In the structure of succinic acid, there are two arms each carrying a carboxylate group that can be used to coordinate metal ions [1-3]. These two carboxylate groups are linked by an alkyl chain that gives the molecule the ability to appear in various conformations: syn−syn, anti−anti, and syn−anti [4]. This ability to arrange itself in different ways in space allows for several coordination modes, including: 1-, 1-2, 2-1-. Chelation and bidentate bridging modes are more common than monodentate coordination [5-10]. The succinate anion can also act as a counterion in coordination complexes [11,12]. In some complexes, the simultaneous presence of succinate as a ligand and a counterion is also found [8,13]. Succinate can also coexist with the neutral molecule succinic acid in the same complex [13,14]. Furthermore, the simultaneous use of succinic acid and an imidazole derivative makes it possible to generate transition metal complexes with interesting structures and properties [15,16]. Supramolecular structures based on significant interactions between co-ligands derived from imidazole and succinate flexibility are reported in the literature [17,18]. In the present work, we have mixed, at the same time, succinic acid, 1-ethyl-2,5-dihydro-1H-imidazole and copper acetate in 1:1:1 ratio to prepare the described and characterized complex.

# Material and methods

## Starting Materials and Instrumentations

Succinic acid, 1-ethyl-2,5-dihydro-1H-imidazole and copper acetate salt were commercial products (from Aldrich) and were used without further purifications. The solvents were of analytical reagent grade and were used directly without further purification. Elemental analyses of C, H and N were recorded on a VxRio EL Instrument. Infrared spectra were obtained on a FTIR Spectrum Two of Perkin Elmer spectrometer in the 4000-400 cm-1 region.

## Synthesis of the complex

0.354 g (3 mmol) of HO₂C(CH)₂CO₂H and 0.588 g (3 mmol) of C₃H₃N₂C₂H₂ were dissolved in 20 mL of distilled water. After obtaining a clear solution, 0.544 g (3 mmol) of Cu(CH₃COO)₂ dissolved in 5 mL of distilled water was added and the mixture was stirred for three hours at room temperature. A blue solution is obtained. This solution is subjected to evaporation of the solvent, which produces blue crystals after a month. Suitable blue single crystals have been characterized by X-ray crystallographic analysis. Yield 56 %. Analysis calculated for [C14H20CuN4O4]: C, 45.22 ; H, 5.42 ; N, 15.07. Found: C, 45.20 ; H, 5.40 ; N, 15.04. FT-IR (, cm-1) : 1706, 1657, 1408, 1391, 881, 840.

## Crystal Structure Determination

“Crystals suitable for single-crystal X-ray diffraction, of the reported compound (1), were grown by slow evaporation of distilled water solution of the complex. Details of the crystal structure solution and refinement are given in Table 1. Diffraction data were collected using a Rigaku FRE+ equipped with Varimax confocal mirrors and UG2 Universal goniometer with graphite monochromatized CuKα radiation (λ = 1.5405 Å). All data were corrected for Lorentz and polarization effects. Complex scattering factors were taken from the program package SHELXTL” [19]. “The structures were solved by direct methods which revealed the position of all non-hydrogen atoms. All the structures were refined on F2 by a full-matrix least-squares procedure using anisotropic displacement parameters for all non-hydrogen atoms [20]. H atoms (NH, OH, CH and CH3 groups) were geometrically optimized and refined as riding models by AFIX instructions. Molecular graphics were generated using ORTEP” [21].

Table 1. Crystallographic data and refinement parameter for the complex (1).

| Chemical formula | C14H20CuN4O4 |
| --- | --- |
| Mr | 371.88 |
| Crystal system | Orthorhombic |
| Space group | P212121 |
| Temperature (K) | 100 |
| a, b, c (Å) | 9.8343 (2) |
| b (Å) | 12.6346 (3) |
| c (Å) | 13.0242 (3) |
| V (Å3) | 1618.29 (6) |
| Z | 4 |
| Radiation type | Cu Kα |
| µ (mm−1) | 2.14 |
| Crystal size (mm) | 0.27 × 0.10 × 0.05 |
| Tmin, Tmax | 0.596, 0.897 |
| No. of measured | 21241 |
| No. of independent | 2968 |
| No. observed [I > 2σ(I)] reflections | 2937 |
| Rint | 0.039 |
| R[F2 > 2σ(F2)] | 0.019 |
| wR(F2) | 0.052 |
| GOF | 1.07 |
| No. of reflections | 2968 |
| No. of parameters | 210 |
| No. of restraints | 0 |
| Δρmax, Δρmin (e Å−3) | 0.21, −0.24 |

# RESULT AND DISCUSSION

### General Studies

The complex is prepared by mixing succinic acid, 1-ethyl-2,5-dihydro-1H-imidazole and copper acetate in 1:1:1 ratio (Scheme 1). The elemental analysis results are in good agreement with the calculated values for the synthesized mononuclear copper(II) complex which is non-hygroscopic and stable in air. The spectrum of succinic acid exhibits a broad O–H stretching band in the region 3300–2500 cm-1, which envelops the C–H stretching bands. This broad O–H stretching band suggests the presence of hydrogen bonding in succinic acid molecules, which may be in dimeric or polymeric form. After the coordination reaction with copper(II), this band disappears from the infrared spectrum of the complex. Significant changes in the position of other bands are also observed when comparing the two spectra. These changes concern the C=O, C–O, and O–H stretching and bending vibration bands in the region 1300–1700 cm-1. In the infrared spectrum of succinic acid, the C=O stretching band is observed at 1676 cm-1, the O–H band at 890 cm-1, and the C–O stretching band at 1304 cm-1. In the infrared spectrum of the copper(II) complex, the broad bands due to the OH groups disappears. The C=O stretching bands shift to low frequencies and appears as intense stretching vibrations band at 1567 cm-1 and a weaker band at 1392 cm-1, which are attributed to the asymmetric (asCOO) and symmetric (sCOO) vibrations, respectively. The difference between  (asCOO -sCOO) is a criterion for determining the coordination mode between the carboxylate group and the metallic ion [22]. The difference  value of 159 cm-1 indicates that the succinate coordinates to the copper(II) ion in a monodentate fashion. At ca.1300 cm-1 there is a peak corresponding to C–O stretching vibrations. In the spectrum of complex, the medium band around 1530 cm-1 is assigned to the vibration mode C=N of the imidazole ring [23].

Scheme 1. Synthetic scheme of the preparation of the complex.

### Structure Description of the Complex

Title compound [Cu(O2C(CH2)2CO2)(C3H5N2C2H5)2] (1) has been synthesized by mixing succinic acid, 1-ethyl-2,5-dihydro-1H-imidazole and copper acetate in 1:1:1 ratio. Single crystals were grown by slow evaporation of an aqueous saturated solution of the copper(II) complex and allowed its structure characterization by X ray diffraction. The compound crystallizes in the orthorhombic system chiral P212121 space group with a = 9.8406(3)Å, b = 12.6318(3)Å, c = 13.0246(4)Å, α = β = γ = 90°, V = 1619.016Å3 and Z = 4. The asymmetric unit is composed of one copper(II) ion tetracoordinated by one oxygen atom of one succinate oxyanion -O2C(CH2)2CO2- in η1-mode and two nitrogen atoms from two neutral 1-ethyl-2,5-dihydro-1H-imidazole molecules acting in η1-mode. Each copper(II) center is coordinated to a succinate oxygen atom from a neighboring molecule complex in η1-mode (Figure 1b). Thus, the copper(II) center situated in a N2O2 site is tetracoordinated and the succinate group acts as a bridge between two CuII ions. The geometry around the tetracoordinated Cu1 ion is determined using the distortion index or the tetragonality parameter [24] which is stated as follows 4 = (360-α-β)/141 (α and β are the two largest angles around the central atom). 4 = 0 designates a perfect square planar geometry and 4 = 1 gives a perfect tetrahedron. The 4 value of 0.028 is indicative of a distorted square planar geometry around Cu1 (Figure 1). In fact, the bond angle values (Table 2) of 90.49(7)° [O1—Cu1—N1], 90.65(7)° [O4i—Cu1—N3], 89.05(7)° [O4i–Cu1–N1], 89.14(7)° [O1—Cu1—N3] are slightly deviated from the ideal value of 90° for a perfect square planar geometry (Table 2). The transoid angle values are 175.47 (7)° [O1—Cu1—O4i] and 171.51 (8)° {N1—Cu1—N3] and deviate from the ideal value of 180°. The sum of the angles subtended by the atoms around Cu1 is 359.33°. The Cu–Osuccinic bond lengths are Cu1–O1 = 1.9567 (16) Å and Cu1—O4i = 1.9741 (15)Å. Similar geometric parameters have also been reported for succinic complexes : [Cu2(C4H4O4)2(C12H12N2)]n, [Cu–O: 1.955 (4)–1.983 (5)Å [25] and [Cu2(C4H4O4)-(NO3)2 (C12H8N2)2(H2O)2], [Cu–O: 1.925 (3)Å [26]. The Cu–Nimidazol bond lengths which are Cu1–N1 = 1.9855 (19) Å and Cu1–N3 = 1.9880 (19) Å are comparable to the values reported for an imidazole complex [27]. In the asymmetric unit of the title complex, there are C2—H2A···O3 and C5—H5···O3, hydrogen-bonding interactions, which act to stabilize the structure by forming S(6) ring. The succinate ligands bridge the CuII centres, forming one-dimensional polymeric chains. The crystal packing (Figure 2) also features symmetry-related intermolecular hydrogen bonds (C7—H7A···O3i, C8—H8···O4ii, C10—H10···O2iii ; symmetry codes as in Table 3), linking the one-dimensional polymeric chains into sheets parallel to the b axis.

Table 2. Selected geometric parameters (Å, °).

| Cu1—O1 | 1.9567 (16) | Cu1—N1 | 1.9855 (19) |
| --- | --- | --- | --- |
| Cu1—O4i | 1.9741 (15) | Cu1—N3 | 1.9880 (19) |
| O1—Cu1—O4i | 175.47 (7) | O1—Cu1—N3 | 89.14 (7) |
| O1—Cu1—N1 | 90.49 (7) | O4i—Cu1—N3 | 90.65 (7) |
| O4i—Cu1—N1 | 89.05 (7) | N1—Cu1—N3 | 171.51 (8) |

Symmetry code: (i) −x+1, y+1/2, −z+3/2.

Figure 1. A view of the title compound, showing the atom-numbering scheme for the asymmetric unit (symmetry codes: (i) −x+1, y+1/2, −z+3/2). Displacement ellipsoids are drawn at the 30% probability level.

Table 3. Hydrogen-bond geometry (Å, °).

| D—H···A | D—H | H···A | D···A | D—H···A |
| --- | --- | --- | --- | --- |
| C2—H2A···O3 | 0.99 | 2.51 | 3.350(3) | 142.1 |
| C5—H5···O3 | 0.95 | 2.46 | 3.171(3) | 131.8 |
| C7—H7A···O3i | 0.99 | 2.50 | 3.089(3) | 118.2 |
| C8—H8···O4ii | 0.95 | 2.43 | 3.313(3) | 154.1 |
| C10—H10···O2iii | 0.95 | 2.29 | 3.165(3) | 152.4 |

Symmetry codes: (i) −x+1, y+1/2, −z+3/2; (ii) x, y+1, z; (iii) −x+1/2, −y+1, z−1/2.

Figure 2. A partial packing plot shows periodic sheets that extend parallel to the b axis.

# Conclusion

In the present work, we report the synthesis and characterization of a new polymeric complex of copper(II) prepared from succinic acid and 1-ethyl-2,5-dihydro-1H-imidazole. The structure of the complex is elucidated by infrared spectroscopy study and X-ray crystallographic analyze. In the copper(II) complex the metal center is tetracoordinated and the metal ion is situated in N2O2 inner. The environment around the Cu(II) ion is best described as square planar geometry. The coordination complex is a polymeric structure, in which each bridging succinate ions acts in 1:2-mode.

# Supporting information

CCDC- 2432731- contains the supplementary crystallographic data for the copper(II), complex. These data can be obtained free of charge via Available https://www.ccdc.cam.ac.uk/ structures/, or by e-mailing data_request@ccdc.cam.ac.uk, or by contacting The Cambridge Crystallographic Data Centre, 12 Union Road, Cambridge CB2 1EZ, UK; fax: +44(0)1223-336033.

# COMPETING INTERESTS DISCLAIMER:

Authors have declared that they have no known competing financial interests OR non-financial interests OR personal relationships that could have appeared to influence the work reported in this paper.

Disclaimer (Artificial intelligence)

Author(s) hereby declare that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc.) and text-to-image generators have been used during the writing or editing of this manuscript.

REFERENCES

- Demir, S., Kantar, G. K., Topcu, Y., & Li, Q. (2012). Solvothermal synthesis and characterization of coordination polymers of cobalt(II) and zinc(II) with succinic acid. Transition Metal Chemistry, 37(3), 257‑263.

Available https://doi.org/10.1007/s11243-012-9581-8

- Junior, J. A. P., Rocchi, A. J. S., Biagioni, B. T., Cavicchioli, M., Machado, R. T. A., Pavan, F. R., Corbi, P. P., Lustri, W. R., Pereira, D. H., & Massabni, A. C. (2021). Chemical, spectroscopic characterization, molecular modeling and antibacterial activity assays of a silver (I) complex with succinic acid. Eclética Química, 46(2), 26-35.

Available https://doi.org/10.26850/1678-4618eqj.v46.2.2021.p26-35

- Skorik, N. A., & Vasil’eva, O. A. (2023). Interaction of Copper(II) with Succinic Acid and Selected Amino Acids. Russian Journal of Inorganic Chemistry, 68(4), 458‑465.

Available https://doi.org/10.1134/S0036023623600211

- Huang, F.-P., Zhang, Q., Yu, Q., Bian, H.-D., Liang, H., Yan, S.-P., Liao, D.-Z., & Cheng, P. (2012). Coordination Assemblies of CoII/NiII/ZnII/CdII with Succinic Acid and Bent Connectors : Structural Diversity and Spin-Canted Antiferromagnetism. Crystal Growth & Design, 12(4), 1890‑1898.

Available https://doi.org/10.1021/cg201577w

- Demir, S., Yilmaz, V. T., Yilmaz, F., & Buyukgungor, O. (2009). One-Dimensional Cobalt(II) and Zinc(II) Succinato Coordination Polymers with Nicotinamide : Synthesis, Structural, Spectroscopic, Fluorescent and Thermal Properties. Journal of Inorganic and Organometallic Polymers and Materials, 19(3), 342‑347.

Available https://doi.org/10.1007/s10904-009-9273-9

- Liu, Y., Zhang, C., Xu, D., Xu, Y., & Lii, G. (2001). Synthesis and Crystal Structure of a Succinatomanganese(II) Complex with Phenanthroline. Journal of Coordination Chemistry, 53(1), 47‑53.

Available https://doi.org/10.1080/00958970108022600

- Kondratenko, Y., Zolotarev, A. A., Ignatyev, I., Ugolkov, V., & Kochina, T. (2020). Synthesis, crystal structure and properties of copper(II) complexes with triethanolamine and carboxylic acids (succinic, salicylic, cinnamic). Transition Metal Chemistry, 45(1), 71‑81.

Available https://doi.org/10.1007/s11243-019-00359-7

- Padmanabhan, M., Kumary, S. M., Huang, X., & Li, J. (2005). Succinate bridged dimeric Cu(II) system containing sandwiched non-coordinating succinate dianion : Crystal structure, spectroscopic and thermal studies of [(phen)2Cu(μ-L)Cu(phen)2]L·12.5H2O (H2L=succinic acid; phen=1,10-phenanthroline). Inorganica Chimica Acta, 358(13), 3537‑3544.

Available https://doi.org/10.1016/j.ica.2005.05.027

- Vučković, G., Antonijević-Nikolić, M., Lis, T., Mroziński, J., Korabik, M., & Radanović, D. D. (2008). X-ray analyses, spectroscopic and magnetic properties of [Cu4(succinato)(tpmc)2](ClO4)6·2C2H5OH·4H2O and [Cu2(C6H5COO)tpmc](ClO4)3·0.5CH3OH·0.5H2O complexes. Journal of Molecular Structure, 872(2), 135‑144.

Available https://doi.org/10.1016/j.molstruc.2007.02.028

- Yilmaz, V. T., Demir, S., Andac, O., & Harrison, W. (2002). Mixed-Ligand Metal Succinate Complexes with 1,10-Phenanthroline and Ethylenediamine : Synthesis, Characterization, Spectroscopic and Thermal Studies. Crystal Structure of Succinatocobalt(II) Complex with Phenanthroline. Journal of Coordination Chemistry, 55(8), 863‑872.

Available https://doi.org/10.1080/0095897022000002196

- Ghosh, A. K., Jana, A. D., Ghoshal, D., Mostafa, G., & Chaudhuri, N. R. (2006). Toward the Recognition of Enolates/Dicarboxylates : Syntheses and X-ray Crystal Structures of Supramolecular Architectures of Zn(II)/Cd(II) Using 2,2‘-Biimidazole. Crystal Growth & Design, 6(3), 701‑707.

Available https://doi.org/10.1021/cg050473n

- Mao, H., Zhang, C., Li, G., Zhang, H., Hou, H., Li, L., Wu, Q., Zhu, Y., & Wang, E. (2004). New types of the flexible self-assembled metal–organic coordination polymers constructed by aliphatic dicarboxylates and rigid bidentate nitrogen ligands. Dalton Transactions, 22, 3918‑3925.

Available https://doi.org/10.1039/B410235E

- Zheng, Y.-Q., Liu, W.-H., & Lin, J.-L. (2002). Two Succinato-bridged Zinc(II) Phenanthroline Complexes : [Zn(phen)L2/2](H2L) and [(phen)2Zn(μ-L)Zn(phen)2]L·11H2O with H2L = Succinic Acid. Zeitschrift für anorganische und allgemeine Chemie, 628(3), 620‑624.

Available https://doi.org/10.1002/1521-3749(200203)628:3<620::AID-ZAAC620>3.0.CO;2-K

- Li, S.-L., Usman, A., Razak, I. A., Rahman, A. A., Fun, H.-K., Wu, J.-Y., Tian, Y.-P., Jiang, M.-H., & Chen, Z.-Y. (2003). Bis(thiosemicarbazido-κ2N,S)nickel(II)–succinate–succinic acid (1/1/1). Acta Crystallographica Section E, 59(4), m199‑m201.

Available https://doi.org/10.1107/S160053680300641X

- Ghosh, A. K., Ghoshal, D., Zangrando, E., & Chaudhuri, N. R. (2007). Synthesis, crystal structure and thermal analysis of supramolecular architectures of copper(II)(2,2′-biimidazole) complexes using dicarboxylate as a coligand. Polyhedron, 26(15), 4195‑4200.

Available https://doi.org/10.1016/j.poly.2007.05.042

- Zheng, Y.-Q., Lin, J.-L., & Ying, E.-B. (2003). New Mixed Ligand Copper(II) Complexes : Syntheses and Crystal Structures of Cu(Imid)2(H2O)L with Imid = Imidazole, L = Succinic and Fumaric Anions. Zeitschrift für anorganische und allgemeine Chemie, 629(4), 673‑676.

Available https://doi.org/10.1002/zaac.200390114

- Liu, Y., Xu, D., Nie, J., Wu, J., & Chiang, M. Y. (2003). Synthesis and Crystal Structure of Bis(Imidazole)(µ-Succinato)Manganese(II). Journal of Coordination Chemistry, 56(3), 155‑159.

Available https://doi.org/10.1080/0095897031000065935

- MacDonald, J. C., Dorrestein, P. C., & Pilley, M. M. (2001). Design of Supramolecular Layers via Self-Assembly of Imidazole and Carboxylic Acids. Crystal Growth & Design, 1(1), 29‑38.

Available https://doi.org/10.1021/cg000008k

- Sheldrick, G. M. (2015a). Acta Crystallographica Section A, 71, 3-8.

Available https://doi.org/10.1107/S2053273314026370

- Sheldrick, G. M. (2015b). Acta Crystallographica Section C, 71, 3-8.

Available https://doi.org/10.1107/S2053229614024218

- Farrugia, L. J. J. Applied. Crystallography, 2012, 45, 849-854

Available https://doi.org/10.1107/S0021889812029111

- Martínez, D., Motevalli, M., & Watkinson, M. (2010). Is there really a diagnostically useful relationship between the carbon–oxygen stretching frequencies in metal carboxylate complexes and their coordination mode? Dalton Transactions, 39(2), 446‑455.

Available https://doi.org/10.1039/B913865J

- Aravind, R., Brahma, G. S., Swain, T., & Sahu, A. K. (2021). Synthesis, characterization of imidazole-based copper complex mixtures and study of their thermal behaviour. International Journal of Energy Research, 45(6), 9179‑9192.

Available https://doi.org/10.1002/er.6445

- Yang, L., Powell, D. R. & Houser, R. P. (2007). Dalton Transactions, 955–964.

Available https://doi.org/10.1039/B617136B

- González Garmendia, M. J., Nacianceno, V. S., Seco, J. M. & Zúñiga, F. J. (2009). Acta Crystallographica Section C, 65, m436–m439.

Available https://doi.org/10.1107/S0108270109040566

- Long, L.-S., Wang, P.-J., Chen, X.-Y., Fang, X.-M. & Ng, S. W. (2001). Acta Crystallographica Section E, 57, m328–m330.

Available https://doi.org/10.1107/S1600536801010571

- Padilha, D. da S. & Scarpellini, M. (2019). Acta Crystallographica Section E, 75, 547–551.

Available https://doi.org/10.1107/S2056989019004055