Nickel borate: A new catalyst for heterocycles synthesis

ABSTRACT

The synthesis of 2,4,5-Triaryl-1H-imidazole derivatives is effectively accomplished via a facile and adaptable multicomponent reaction pathway. This process, catalysed by Nickel (II) borate in Acetone, involves the reaction of a 1,2-dicarbonyl compound, an aromatic aldehyde, and ammonium acetate, which functions as the in-situ ammonia source. This approach offers advantages which include simple workup, moderate to high reaction rate and satisfactory product yields.

Keywords: 2,4,5-Triaryl-1H-imidazole, multicomponent reaction, Nickel (II) borate, simple workup, satisfactory product yields.

1. INTRODUCTION

Heterocyclic compounds are cyclic organic compounds showing presence of one or more atoms of elements other than atoms of basic element that is carbon. Most of the Heterocyclic compounds contain Nitrogen, Oxygen or Sulphur as the part of ring system.[1] The research has established that natural and synthetic Heterocyclic compounds possess medicinal properties.[2] This has been proved to be an encouraging factor to the ongoing research in the field of Heterocyclic compounds.

Even if several Heterocyclic compounds exist, those with nitrogen as heteroatom held the prime place.[3] Due to the diverse biological activities, development of the systematic synthesis of nitrogen-containing heterocyclic compounds has been the subject of interest for the researchers all over the world.[4]

Among the several Heterocyclic compounds, Triarylimidazoles are found to be unique one as these structural units provide biological activities to many natural as well as synthetic organic compounds.[5] Further, the herbicidal [6], fungicidal [7], anti-cancer [8], antithrombotic nature [9], antiwear [10] and many other biological activities of Triaryl imidazole derivatives [11] have been well explained in the literature. Due to this, Triarylimidazoles have attracted attention of researchers resulting in development of several methodologies for their synthesis.

Triarylimidazoles are generally prepared using Multicomponent pathway.[12] Metal salts in different forms have been used; for example, Nickel Chloride, Ceric ammonium nitrate, Zirconyl Chloride, Uranyl Nitrate, MnO2-FeSO4, Mn2+ Complex of [7-Hydroxy-4-methyl-8-coumarinyl] Glycine.[13] Silica based catalysts such as Silica Chloride, Sulfuric acid immobilized on silica gel are also reported for the synthesis of Triarylimidazoles.[14] Ionic liquid based catalyst systems are found to be effective.[15] The other protocols include PEG-400, Fe3O4@ SiO2-ABMA-MnCl2 nanocomposite, Co (ii)–Cu (ii) mixed-oxide, Sulphated tin oxide, molecular sieve supported titanium catalyst.[16] Some green protocols used Glutamic Acid, Lemon Juice, Nano ZnS‐ZnFe2O4.[17]

In the field of Organic synthesis, nickel compounds occupy prime position due to their catalytic efficacy which is consistently highlighted throughout the relevant literature.[18] The present research work would be communicating the catalytic application of Nickel (II) borate [Ni3(BO3)2] in a synthetic protocol to prepare 2,4,5-Triaryl-1H-Imidazoles. (Scheme 1)

Scheme 1. 2,4,5-Triaryl-1H-Imidazoles

2. MATERIALS AND EXPERIMENTAL DETAILS

Chemicals procured from Sigma-Aldrich and Merck were used without further purification. Melting points were determined using the open capillary method with a Thiele's tube. Thin layer chromatography (TLC) was employed to assess the reaction completion. The system used consisted of a mixture of Pet ether and Ethyl acetate in required proportions. The crude products were purified using recrystallization with suitable solvent. The formation of the 2,4,5-triaryl-1H-imidazoles was proved by the agreement between their melting points and previously reported values in the literature.

General procedure

A reaction mixture comprised of Benzil (0.210 gm,1mmol), an aromatic aldehyde (1mmol), and ammonium acetate (0.154 gm, 2 mmol) in Acetone as solvent (5.0 mL) was prepared. Nickel (II) borate (0.2 mmol) was then added to serve as catalyst in the reaction. Thorough mixing of the reaction contents was ensured by employing a magnetic stirrer equipped with a magnetic needle at room temperature (around 260C to 270C). Upon the completion of reaction as confirmed using TLC, the reaction mixture was filtered to remove the heterogeneous catalyst. The collected filtrate was then carefully transferred into a beaker of cold water (10 mL) for solidification of product. Washing with cold water followed by recrystallization from hot ethanol gave the purified product. The prepared 2,4,5-triaryl-1H-imidazoles were characterized by melting point data.

The Optimal experimental parameters for the synthesis of 2,4,5-Triaryl-1H-imidazole derivatives were elucidated by selecting reaction involving Benzil, Benzaldehyde, and Ammonium acetate as a model reaction (Scheme 2).

Scheme 2. Synthesis of 2,4,5-Triaryl-1H-imidazole derivatives from Benzil, Benzaldehyde, and Ammonium acetate

The selection of suitable solvent for the reaction was done performing the model reaction in a series of solvents and analysing its effect on reaction time and product yield. Initially, the model reaction was performed in non-polar solvents like CCl4, CH2Cl2, CHCl3. Further, it was performed with polar solvent like CH3CN, C2H5OH, Acetone, DMF, DMSO and H2O. On the basis of analysis of data for reaction time and product yield received with different solvents, Acetone was found to be the most appropriate solvent for the reaction (Table 1, Entry 9).

Table 1. Section of solvent for the synthesis of 2, 4, 5-Triaryl-1H-imidazole (1a)

| Entry | Catalyst | Solvent | Reaction Time (Minutes) | Yielda (%) |
| --- | --- | --- | --- | --- |
| 1 | Ni3(BO3)2 | CCl4 | 180 | Less than 5 |
| 2 | Ni3(BO3)2 | CH2Cl2 | 120 | 20 |
| 3 | Ni3(BO3)2 | CHCl3 | 240 | 20 |
| 4 | Ni3(BO3)2 | CH3CN | 150 | 40 |
| 5 | Ni3(BO3)2 | DMF | 110 | 39 |
| 6 | Ni3(BO3)2 | DMSO | 120 | 55 |
| 7 | Ni3(BO3)2 | C2H5OH | 80 | 45 |
| 8 | Ni3(BO3)2 | Acetone | 50 | 88 |
| 9 | Ni3(BO3)2 | H2O | 70 | 35 |

aIsolated Yields

The further investigation involved finding out optimal catalyst load (Table 2, Entry1 to 6). The data mentioned in Table 2 demonstrates that 0.2 mmol of the catalyst could gave maximum yield of 2,4,5-Triaryl-1H-imidazole (1a) in 52 minutes. An increase in the yield of product was not observed with further increment in catalyst load.

Table 2. Optimal catalyst load for the synthesis of 2, 4, 5-Triaryl-1H-imidazole (1a) in Acetone

| Entry | Catalyst (mmol) | Reaction Time (Minutes) | Yielda (%) |
| --- | --- | --- | --- |
| 1 | 0.01 | 120 | 49 |
| 2 | 0.05 | 90 | 65 |
| 3 | 0.1 | 86 | 69 |
| 4 | 0.2 | 52 | 89 |
| 5 | 0.3 | 54 | 88 |
| 6 | 0.4 | 52 | 89 |

aIsolated Yields

3. RESULTS AND DISCUSSION

The applicability of reaction for the synthesis of 2,4,5-Triaryl-1H-imidazoles was evaluated through the investigation of the reaction of Benzil with a range of aromatic aldehydes and ammonium acetate under the previously optimized conditions. (Table 3, 1a-j)

The catalytic efficacy of Ni3(BO3)2 in Acetone has been successfully proved as it smoothly facilitated the reaction between Benzil, Aldehyde and Ammonium acetate to form 2,4,5-Triaryl-1H-Imidazoles (Table 3). The reaction has occurred under mild conditions with moderate to good yields of products. As a Lewis acid, Ni3(BO3)2 proved to be an efficient catalyst under mild conditions with moderate to good yields.  Ni3(BO3)2 as a Lewis acid was found to be reacting well with various aromatic aldehydes irrespective of their electronic nature or substitution pattern (Table 3).

Reaction rate and yield of products were significantly influenced by the nature and position of substituents on Aromatic aldehydes. Electron-withdrawing substituents must be stabilizing the transition state due to which Aromatic aldehydes bearing such groups consistently afforded the high yields within the shortest reaction duration (Table 3, Entries 1e,1g,1h, 1i). In contrast, the presence of electron-donating substituents led to a decrease in product yield and an increase of the reaction rate (Table 3, Entries 1b, 1c). The reduced reactivity of aromatic aldehydes with ortho-substituent suggests a significant steric hindrance effect near to reaction site (Table 3, Entries 1d, 1j). Notably, aliphatic aldehydes were completely unreactive under the employed conditions highlighting the specific requirements for an aromatic system in this transformation.

Table 3. Synthesis of 2,4,5-Triaryl-1H-imidazoles (1a-j) *

| Entry | R- | Product | Time (minutes) | Yielda (%) | Melting Point (0C) (Literature value) |
| --- | --- | --- | --- | --- | --- |
| 1 | H | [2,4,5-Triphenyl-1H-imidazole] (1a) | 52 | 88-89 | 266-267 (267–269)19 |
| 2 | 4-CH3 | [2-(p-tolyl)-4, 5-diphenyl-1H-imidazole] (1b) | 60 | 77 | 228 (227-229)20 |
| 3 | 4-OCH3 | [2-(p-methoxyphenyl)-4, 5-diphenyl-1H-imidazole] (1c) | 70 | 72 | 221-222 (220–223)19 |
| 4 | 2-OCH3 | [2-(o-methoxyphenyl)-4, 5-diphenyl-1H-imidazole] (1d) | 80 | 65 | 209-210 (210-211)13d |
| 5 | 4-Cl | [2-(p-chlorophenyl)-4, 5-diphenyl-1H-imidazole] (1e) | 48 | 88 | 263 (262–264)19 |
| 6 | 2-Cl | [2-(o-chlorophenyl)-4, 5-diphenyl-1H-imidazole] (1f) | 44 | 85 | 187-188 (186-190)20 |
| 7 | 4-OH | [2-(p-hydroxyphenyl)-4, 5-diphenyl-1H-imidazole] (1g) | 42 | 90 | 231 (232–233)19 |
| 8 | 4-Br | [2-(p-bromophenyl)-4, 5-diphenyl-1H-imidazole] (1h) | 45 | 88 | 249-250 (248-249)21 |
| 9 | 4-NO2 | [2-(p-nitrophenyl)-4, 5-diphenyl-1H-imidazole] (1i) | 40 | 90 | 235-236 (235–238)22 |
| 10 | 3-NO2 | [2-(o-nitrophenyl)-4, 5-diphenyl-1H-imidazole] (1j) | 45 | 87 | 231 (230–231)19 |

*Reaction condition: Benzil (1.0 mmol), aldehyde (1.0 mmol), ammonium acetate (2mmol), Ni3(BO3)2 (0.2 mmol) in Aetone (5.0 mL) at Room Temperature (around 260C to 270C), aIsolated Yields

The catalyst Nickel (II) borate was found to be a heterogeneous and easily separable from the reaction mixture which encouraged to check its reusability. After separation from the reaction mixture, it was washed with Acetone and used for the next runs of the synthesis. Nickel (II) borate sustained its catalytic activity in performing the preparation of the desired 2,4,5-Triaryl-1H-imidazole derivatives for the three runs (Table 4).

Table 4 Study of reusability of Nickel (II) borate in the synthesis of 2,4,5-Triphenyl-1H-imidazole (1a) *

| Run No. | 1 | 2 | 3 | 4 | 5 |
| --- | --- | --- | --- | --- | --- |
| Time (Minutes) | 52 | 65 | 80 | 120 | More than 120 |
| Yielda (%) | 88-89 | 72 | 52 | 20 | 10 |

*Reaction condition: Benzil (1.0 mmol), Benzaldehyde (1.0 mmol), ammonium acetate (2mmol), Ni3(BO3)2 (0.2 mmol) in Aetone (5.0 mL) at Room Temperature (around 260C to 270C), aIsolated Yields

Thus, Nickel (II) borate was found to be a reusable catalyst for the synthesis of 2,4,5-Triaryl-1H-imidazole derivatives which adds to its value as Green catalytic material for synthesis of other heterocycles also.

MECHANISM (Scheme 3)

On the basis of findings, a plausible mechanism can be proposed.[23] Accordingly, it seems that the catalyst must have activated both an aromatic aldehyde and Benzil via coordinating with oxygen atom of carbonyl group which was followed by nucleophilic attack of ammonia molecule to form Imine intermediates (A and B). Further, Imine intermediate (B) activated by the catalyst reacted with Imine intermediate (A) and finally gave desired product(1a-j).

Scheme 3. Mechanism

CONCLUSION

The use of Ni3(BO3)2 as a catalyst in Acetone presents a highly advantageous protocol for synthesizing 2,4,5-Triaryl-1H-imidazoles via a one-pot, three-component reaction. This catalyst offers good performance along with other benefits including easy separation due to its heterogeneous nature, cost-effectiveness and ready availability. The use of Ni3(BO3)2 as a catalyst facilitates smooth reactions with various aromatic aldehydes, achieving good yields of the target imidazole derivatives in a short duration. Further, the catalyst was effective in small quantity (0.2mmol) to carry out transformations.

Disclaimer (Artificial intelligence): Author hereby declares that NO generative technologies such as Large Language Models (ChatGPT, COPILOT etc.) and text-to-text generators have been used during the writing or editing of this manuscript.

REFERENCES

[1] Achar, K. C., Hosamani, K. M., Seetharamareddy, H. R.  (2010).  In-vivo analgesic and anti- inflammatory activities of newly synthesized benzimidazole derivatives.  European journal of medicinal chemistry, 45(5), 2048-54.

[2] Hossain, M., Nanda, A. K.  (2018).  A review on heterocyclic: synthesis and their application in medicinal chemistry of imidazole moiety. Science. 6(5), 83-94.

[3] Ye, Z., Zhang, F. (2019). Recent Advances in Constructing Nitrogen‐Containing Heterocycles via Electrochemical Dehydrogenation. Chinese Journal of Chemistry, 37(5), 513-28.

[4] Heers, J., Backx, L. J. J., Mostmans, J. H., Van, C. J. (1979). Synthesis and analgesic properties of 1,2,3,4-tetrahydroisoquinolines. Journal of Medicinal Chemistry, 1979: 22(8): 1003-1005.

[5] Soni, J., Sethiya, A., Sahiba, N., Agarwal, D.K., Agarwal, S. (2019). Contemporary progress in the synthetic strategies of imidazole and its biological activities. Current Organic Synthesis, 16(8),1078-104.

[6] Liebl, R., Randte, R., Mildenberger, H., Bauer, K., Bieringer, H. (1987). 1,2,3,4-tetrahydroisoquinoline-3-carboxylic acid: An inhibitor of phenylalanine hydroxylase. Chemical Abstracts, 108, 6018.

[7] Pozherskii, A. F, Soldatenkov, A. T, Katritzky, A. Y. (1997). Heterocycles in Life and Society. Wiley.

[8] (a) Tseng, C.H., Li, C.Y., Chiu, C.C., Hu, H.T., Han, C.H., Chen, Y.L. and Tzeng, C.C. (2012). Combretastatin A-4 derivatives:synthesis and evaluation of 2, 4, 5-triaryl-1 H-imidazoles as potential agents against H1299 (non-small cell lung cancer cell). Molecular diversity, 16(4), 697-709. (b) Elahian, F., Akbari, M., Ghasemi, M., Behtooee, N., Taheri, M. and Amini, M. (2014). Synthesis and anticancer activity of 2, 4, 5-triaryl imidazole derivatives. Letters in Drug Design & Discovery, 11(7), 40-843.

[9] Phillips, A. P., White, H. L., Rosen, S. (1983). Antithrombotic triphenylimidazoles. Chemical Abstracts, 98, 53894z.

[10] Singh, P., Dubey, R., Tiwari, S., Khanna, R.S. and Tewari, A.K. (2015). Triarylimidazoles as potent antiwear agents: Eco-friendly synthesis and materialistic approach. Scientia Iranica, 22(3), 925-933.

[11] (a) Bellina, F., Cauteruccio, S., Rossi, R. (2007). Synthesis and biological activity of vicinal diaryl-substituted 1H-imidazoles. Tetrahedron, 28, 63(22), 4571-624. (b) Zarghi, A., Arfaei, S., Shirazi, F. H. (2013). Design, synthesis, and cytotoxic activities of new 2, 4, 5-triarylimidazoles. Medicinal Chemistry Research, 22(8), 3897-904.

[12] (a) Yang, C., Ren W., Feifei Ba, Junli, H., Aishun, D., Mingdong, Z., Hao G. (2017). Synthesis of 2,4,5-triarylated imidazoles via three-component domino reaction under catalyst-free conditions. Journal of Saudi Chemical Society, 21, 76-81. (b) Durai Ananda Kumar, T., Yamini, N., Subrahmanyam, C. V. S. & Satyanarayana, K. (2014). Design and Optimization of Ecofriendly One-Pot Synthesis of 2,4,5-Triaryl-1H-imidazoles by Three-Component Condensation Using Response Surface Methodology. Synthetic Communications, An International Journal for Rapid Communication of Synthetic Organic Chemistry, 44:15, 2256-2268.

[13] (a) Heravi, M.M., Bakhtiari, K., Oskooie, H.A., Taheri, S.H. (2007). Synthesis of 2,4,5-triaryl-imidazoles catalyzed by NiCl2·6H2O under heterogeneous system. J. Mol. Catal. A: Chem., 263, 279-281. (b) Sangshetti, J. N., Kokare, N. D., Kotharkara, S. A. and Shinde, D. B. (2008). Ceric ammonium nitrate catalysed three component one-pot efficient synthesis of 2, 4, 5-triaryl-1H-imidazoles. Journal of Chemical. Sciences, 120(5), 463–467. (c) Sangshetti, J.N., Kokare, N.D., Kotharkar, S.A. and Shinde, D.B. (2008). ZrOCl2· 8H2O catalyzed one-pot synthesis of 2, 4, 5-triaryl-1H-imidazoles and substituted 1, 4-di (4, 5-diphenylimidazol-yl) benzene. Chinese Chemical Letters, 19(7), 762-766. (d) Sangshetti, J.N., Kokare, N.D., Kotharkar, S.A., Shinde, D.B. (2008). Sodium Bisulfite as an efficient and inexpensive catalyst for the one-pot synthesis of 2, 4, 5-triaryl-1 H-imidazoles from benzil or benzoin and aromatic aldehydes. Monatshefte für Chemie-Chemical Monthly, 139(2), 125-7. (e) Satyanarayana, V.S., Sivakumar, A. (2011). An efficient and novel one-pot synthesis of 2, 4, 5-triaryl-1 H-imidazoles catalyzed by UO2 (NO3)2· 6H2O under heterogeneous conditions. Chemical Papers, 65(4), 519-26. (f) Raheem, A. A., Saleh, A.T. (2021). Multicomponent Reactions Synthesis of Triaryl-1H Imidazoles Using Reductive-oxidative Reactions by MnO2-FeSO4 as a Catalyst. Journal of Chemical Health Risks, 11(2). (g) Sharghi, H., Razavi, S. F., Aberi, M. (2022). One-Pot Three-Component Synthesis of 2, 4, 5-Triaryl-1 H-imidazoles Using Mn2+ Complex of [7-Hydroxy-4-methyl-8-coumarinyl] Glycine as a Heterogeneous Catalyst. Catalysis Letters,152(6), 1769-83.

[14] (a) Chavan, H. V., Narale, D. K. (2014). Synthesis of 2,4,5-triaryl and 1,2,4,5-tetraaryl imidazoles using silica chloride as an efficient and recyclable catalyst under solvent-free conditions. Comptes Rendus Chimie, 17(10), 980-984. (b) Maleki, B., Shirvan, H. K., Taimazi, F., Akbarzadeh, E. (2012). Sulfuric acid immobilized on silica gel as highly efficient and heterogeneous catalyst for the one-pot synthesis of 2, 4, 5-triaryl-1H-imidazoles. International Journal of Organic Chemistry, 2(1):93-9.

[15] (a) Xiaocui, D., Zhou, Z., Zhang, A. and Xie. G. (2013). Brønsted acid ionic liquid [Et3NH][HSO4] as an efficient and reusable catalyst for the synthesis of 2, 4, 5-triaryl-1H-imidazoles. Research on Chemical Intermediates, 39(3), 1101-1108. (b) Borge, V. V., Manjare, S. B., Bangade, V. M., Babre, A. A., Mohite, S. S., Popatkar, B. B. (2025). Trihexyltetradecylphosphonium bis (2, 4, 4-trimethylpentyl) phosphinate Ionic Liquid: An Efficient Catalyst for the Synthesis of 2, 4, 5-triaryl-1H-imidazole Derivatives. Letters in Organic Chemistry, 22, doi: 10.2174/0115701786396536250519043722.

[16] (a) Wang, X. C., Gong, H. P., Quan, Z. J., Li, L., Ye, H.L. (2009). PEG-400 as an efficient reaction medium for the synthesis of 2, 4, 5-triaryl-1H-imidazoles and 1, 2, 4, 5-tetraaryl-1H-imidazoles. Chinese Chemical Letters, 20 (1), 44-47 (b) Alalaq, I. S., Ruaa S., Usama S. A., Ali S. O. K. A., Abeer M. J., Mohammed K. A., et al. (2025). A sustainable approach for synthesis of 2, 4, 5-triaryl-1H-imidazoles using Fe3O4@ SiO2-ABMA-MnCl2 nanocomposite. Research on Chemical Intermediates, 51(3), 1273-1295. (c) Jopale, M. K., Zheng, Z., Choi, S., Shelke, B. N., Mharsale, N., Patil, S., et al. (2024). Co (ii)–Cu (ii) mixed-oxide catalysts for single-step synthesis of 2, 4, 5-triaryl-1 H-imidazole derivatives under microwave irradiation. Dalton Transactions, 53(36), 15284-96. (d) Dake, S. A., Khedkar, M. B., Irmale, G. S., Ukalgaonkar, S. J., Thorat, V. V., Shintre, S. A. and Pawar, R. P. (2012). Sulfated tin oxide: a reusable and highly efficient heterogeneous catalyst for the synthesis of 2, 4, 5-triaryl-1 H-imidazole derivatives. Synthetic Communications, 42(10), 1509-1520. (e) Magyar, Á., Hell, Z. (2019). One-pot three-component synthesis of 2, 4, 5-triaryl-1H-imidazoles in the presence of a molecular sieve supported titanium catalyst under mild basic conditions. Synlett. 30(01), 89-93.

[17] (a) Ankush, B. P., Shitole, B. V., Shitole, N. V. (2021). One-Pot Synthesis of 2,4,5-Triaryl-1H-imidazoles Using Glutamic Acid as Catalyst. Orbital: Electron. J. Chem. 13(3), 232-235. (b) Khan, F. A. K., Shaikh, K. A., Choudhary, J. M., Khan, S. M. I., Shalgar, L. G., Ali, A. and Mateen, S. (2022). Green Chemistry Approach for the Synthesis of 2,4,5-Triaryl-1H-Imidazole Derivatives Using Lemon Juice As a Bio-Catalyst. Journal of Innovations in Pharmaceutical and Biological Sciences, 9(4), 13-17 (c) Varzi, Z., Maleki, A. (2019). Design and preparation of ZnS‐ZnFe2O4: a green and efficient hybrid nanocatalyst for the multicomponent synthesis of 2,4,5‐triaryl‐1H‐ imidazoles. Appl Organometal Chem. 33: e5008.

[18] (a) Ananikov, V. P. (2015). Nickel: The “Spirited Horse” of Transition Metal Catalysis, ACS Catal. 5, 1964−1971 (b) Sabatier, P. (1922). Catalysis in Organic Chemistry; D. Van Nostrand Company: New York, p 15.

[19] Samai, S., Nandi, G. C., Singh, P., Singh, M. S. (2009). L-proline: An efficient catalyst for the one-pot synthesis of 2,4,5-trisubstituted and 1,2,4,5-tetrasubstituted imidazoles. Tetrahedron, 65(49), 10155.

[20] Bamoniri, A., Mirjalili, B. F., Nazemian, S., Mahabadi, N. Y. (2014). Nano silica phosphoric acid as an efficient catalyst for one-pot synthesis of 2,4,5-tri-substituted imidazoles under solvent free condition. Bulgarian Chemical Communications, 46(1), 79-84.

[21] Siddiqui, S. A., Narkhede, U. C., Palimkar, S. S., Daniel, T., Lahoti, R. J., Srinivasan, K. V.  (2005). Room temperature ionic liquid promoted improved and rapid synthesis of 2,4,5-triaryl imidazoles from aryl aldehydes and 1,2-diketones or α-hydroxyketone. Tetrahedron, 61(14), 3539-3546.

[22] Usyatinsky, A. Y., Khmelnitsky, Y. L. (2000). Microwave-assisted synthesis of substituted imidazoles on a solid support under solvent-free conditions. Tetrahedron Letter, 41(26), 5031- 5034.

[23] (a) Varzi, Z., Maleki, Ali, M. (2019). Design and preparation of ZnS‐ZnFe2O4: a green and efficient hybrid nanocatalyst for the multicomponent synthesis of 2,4,5‐triaryl‐1H‐imidazoles. Applied Organometallic Chemistry, 33. 10.1002/aoc.5008. (b) Banazadeh, M., Amirnejat, S., Javanshir, S. Synthesis, Characterization, and Catalytic Properties of Magnetic Fe3O4@FU: A Heterogeneous Nanostructured Mesoporous Bio-Based Catalyst for the Synthesis of Imidazole Derivatives. (2020). Front Chem., 1;8:596029. doi: 10.3389/fchem.2020.596029