Original Research Article

Bond characteristics of coated reinforcing steel bars with reference to deformation of concrete beams

Abstract

A major cause of reinforced concrete deterioration especially in coastal and moist prone areas is corrosion. It has become a threat to reinforced concrete structural integrity throughout the service life of the structural member, and it calls for endless remedial activities with its accompanying economic and safety implications. Expensive remedial measures- galvanization, epoxy coating and fiber-reinforce polymers - are used to prevent corrosion as approved by previous studies. The present study explored the use of cost effective oil paint brands (mat, red-oxide and gloss Leyland paints in Ghana) to variably coat reinforcing steel bars to ascertain their bond strength in concrete while preventing corrosion. There were zero, one, two and three coats averaging 72 µm, 129 µm and 220 µm film thickness of 1-coat, 2-coat and 3-coat respectively for exploration. Double pull-out test was conducted on 120 concrete prisms (size 150 x 150 x 200 mm), centrally reinforced with coated rebars. Loading rate of 0.5kN/s was adopted and data was processed and analyzed by one-way ANOVA. The results indicated that no significant difference exist between paint coated and uncoated reinforcing steel bars on local bond and slip quality for all the selected paint brands used in this study. Though facially, one-coat of paint showed better bonding (18%) quality over zero-coat, two-coat and three-coat were at par with zero-coat, indicating decreasing bond with increasing coat. But reinforcing bar type and size were not affected by the coating. The implication is that the selected oil paint brands would not adversely affect local bond strength, and hence cracking and deflections in concrete when they are used to coat reinforcing bar to prevent corrosion, and therefore recommended for application to reduce maintenance cost.

Keywords: Corrosion, paint coating, local bond strength, slip, number of coating number/type, rebar type/size.

1.  Introduction

Corrosion of reinforcing steel bar becomes a threat to the integrity of the reinforced concrete structures (bridges, buildings, airport runway pavements, water tanks, among others) during the period of its service life (Akortia et al., 2024). When it strikes, it calls for frequent countless remedial activities, because, the rebar tend to expand with pressure overtime beyond the tensile strength of the concrete. This leads to bond reduction, and in severe cases causes the concrete to develop cracks, spall and collapse. Charles et al. (2018) found the corrosion of reinforcing steel bar in concrete as one of the foremost influences to failure of steel and concrete, leading to the use of epoxy and resin/exudate to prevent corrosion effect on reinforcing steel bar. Earlier, Auyeung et al. (2000) indicated that bond strength dilapidation of an unconstrained concrete specimen with a corroded reinforcing steel of 2% could result in a bond loss of 80%, and it is more critical to cross-sectional loss.  That can be very devastating to rebar and the concrete structure at whole and it is a global concern (Rodrigues et al., 2021; and Biparva, 2019). The condition is prevalent with structures along coastal regions, acid rain regions, industrial zones, water-containing structures and structures spanning over river bodies (Akortia et al., 2024). It is a global concern because of its financial implication, if not prevented. According to National Association of Corrosion Engineers (NACE, 2017; Prasad, 2021), corrosion causes annual loss of USD 2.5 trillion globally. This calls for aggressive corrosion protection.

However, the exudates and the epoxy employed and coats used to prevent reinforcing steel corrosion are not without problem. Apart from their scarcity on the local market in West Africa, they also alter the rebar surface against the bond components (mechanical interlock, friction and chemical adhesion) between rebar and concrete. Naha et al. (2021) established that epoxy-coated bars exhibited approximately 18 % lower bond capacity in splitting failures and 25 % lower in pull-out failures relative to uncoated bars. This reduction was attributed to the barrier effect of the coating, which diminishes mechanical interlock and friction at the steel–concrete interface. Similarly, Chen and Wu (2019) found that polymer coatings cut peak bond stress by 20 %, lowering cracking moment by 10 % and boosting service deflection by 15 %, while ultimate moment dipped only 3 %. Crack spacing remained similar, but crack widths grew by 12 %. Hence, the act of preventing corrosion must consider cost effectiveness and the surface quality for good bond stress. Other prevention measures like galvanization and sand blasting are equally expensive and require heavy machinery and energy to achieve, with sand blasting producing a lot of pollution (Buchheit, 2018; Nguyen and Nguyen, 2018). The current study aimed at demonstrating experimentally the use of oil paints (Leyland Brands of red-oxide, matt black and gloss green) produced in Ghana to prevent or delay corrosion of reinforcing steel bars in concrete without compromising good bond stress for structural integrity and safety. The corrosion protection of the paint has been tested and published earlier (Akortia et al., 2024). This paper focused on determining the local bond stress capacity of paint coated mild and high yield steel rebars in concrete, when using the selected paints to prevent corrosion.

2. Materials and method

A total of 120 concrete prism specimens of size 150mm x 150mm x 200mm centrally reinforced, were cast in the study to test local bond strength/stress of the coated rebars against uncoated – control. Hence the internal dimensions of the mould box were 150mm x 150mm x 200mm. These dimensions were selected to represent a prism that is typically within an average flexural cracking length of a beam section/zone in tension.

Table 1: Properties of control test specimens, rebars and aggregates used

| Specimens/material | Size (mm) | Weight (Kg) | Service strength (N/mm2) | Strength (N/mm2) |
| --- | --- | --- | --- | --- |
| Cube | 150 x 150 x 150 | 8.6 |  | 23.1 |
| Cylinder | 150 x 300 | 12.4 |  | 6.6 |
| Prism | 100 x 100 x 500 | 12.5 |  | 4.7 |
| High yield steel | Y12/Y16 |  | 250 | 420 |
| Mild steel | R12/R16 |  | 140 | 250 |
| Chippings | < 14 |  |  |  |
| Sand | < 5 |  |  |  |

2.1 Materials and Equipment

Materials used in this study included graded crushed granite chippings not more than 14mm, pit sand (see Fig. 1 for particle distribution) and ordinary Portland limestone cement grade 32.5 R as the main materials for the concrete work; plywood was used for fabricating the mould box; reinforcing steel bars of sizes 16mm and 12mm, both mild and high yield steel bars (service strength 140N/mm2 and 250N/mm2; yield strength 250N/mm2 and 420N/mm2 respectively – Table 1), and Leylac mat, Leylac red-oxide (guard) and Leylac gloss oil base paints. A concrete mixer, wheel barrow and other mixing tools and double pull-out universal machine, holding tool – ‘VEJ’, dial gauges (precision was 0.01 mm), scale were the equipment used. The water used in the process conformed to BS EN 1008(2002) standard.

b

a

Fig. 1 Particle size distribution of aggregates

2.2 Experimental Methods

2.2.1 Specimens preparation and testing

The steel bars were cut into 120 pieces of length 620mm, and pretreated in conformity with ASTM A 775/A 775M – 01, by cleaning with metal brush and thinner to remove dirt, grease/oil substance and metal oxide from the surface of the steel bar. They were then cleaned with potable water, wiped with cotton rag and dried before coating with brush. The centers were drilled to receive tight transverse 75mm anchor bars to serve as the reference point of the stress and slip that would occur during the double pull-out test and represent point midway between two adjacent cracks in a beam. For each case, the coating was 0, 1, 2, and 3 groups. The control specimens received no coating after the surface preparation. However, the other test specimens received 1, 2, or 3 coats of the various paint types by brush. After selecting the control specimens, all the test specimens received one coat each in their various groups and allowed to dry for 24 hours. Then one coat specimens were taken out and the rest received second coat and allowed to dry for 24 hours. The same step was repeated for the third coat and they were cured under room temperature for 14 days before the bond specimens were cast. Meanwhile the physical properties were taken to determine the coating thickness with digital veneer caliper. Average thickness taken from the web were 72 µm, 129 µm and 220 µm for 1-coat, 2-coat and 3-coat respectively in accordance to ASTM A775/A775 M, section A 1.2 (coating requirement). The varied thicknesses were chosen because coating thickness has effect on bond strength. Hence, that would guide suitable thickness of coating to recommend.

This stage was followed by fixing the rebars in the mould box in order to cast the bond prism specimens. Concrete (mix ratio 1:1.5:3 by weight) was prepared from the above materials with water cement ratio of 0.55 targeting C25 strength, using a mechanical concrete mixer for consistency. Concrete moulds which had been lubricated to facilitate removal were filled in 3 layers, where each layer received tamping compaction of 36 strokes before the next layer (see fig. 3c). After tamping the last layer, the surface was levelled with trowel and allow to set and dry in the open for 24 hours before the moulds were removed. Control test specimens - cubes, cylinders and prisms - were also cast for testing. Workability test resulted in 21mm slump that corresponded to the water cement ratio of 0.55 (see Fig. 3b). The specimens were removed after 24 hours of casting, carefully arranged and covered in the open weather with damp jute sack for curing. Water was applied by pouring each morning and evening for 28 days (see Fig. 3d&e). This process was to enable the concrete attain its strength gradually. They were then cleaned and sent to the laboratory after 28 days for various tests.

2.2.2	Double pull-out Test

The double pull-out test was conducted on the bond specimens using a universal machine (Avery-Denison’s classic 500kN T-series - T42B/C model). Other tools and instruments involved were 4 dial-gauges, camera, VEJ which held the dial gauge to the rebar before testing. Each specimen had two projected rebars fit into the upper and lower grip of the universal machine after fixing the dial gauges. Loading was done incrementally at 2kN intervals to measure the local bond at each load increment. The 16mm high yield specimens were loaded at 5kN interval due to the high service stress at the rebar. The loading was done such that both the rebar and the concrete were in tension. The loading, irrespective of interval was at the rate of 1mm/min or 0.5kN/s (ASTM A944). A pair of two dial gauge readings were taken at the top while another pair at the bottom. The average reading of the two readings in each case was used for analysis of slip. This was meant to reduce error level if just one gauge is used.

The specimens were tested within the service limit of the particular rebar-12mm or 16mm, high yield steel or mild steel rebar. The service limit was calculated based on the strength (140N/mm2 and 250N/mm2 for mild and high yield steel respectively) and the actual cross-sectional area of the rebars. Hence, the local bond maximum pull-out load for the various rebars were 15kN, 26kN, 36kN and 65kN for 12mm mild steel, 16mm mild steel, 12mm high yield steel and 16mm high steel respectively. Fig. 4 show the set-up for the bond test.

2.3 Analysis

The results were illustrated graphically by presenting the bond stress–slip relationship curves and statistically analyzed using analysis of variance (ANOVA) on the computed bond stress and slip values of the test specimens; since the values are on scale, and in order to ascertain the degree of variation that were seen in the data from the various groups.

2.3.1 Local bond

The local bond was calculated based on the recorded bar slip and distance along bar in the three-dimensional formulae proposed by Kankam (1997, 2003). From the formulae, the average bond stress was determined along the continuous rebar in the concrete at each level of bond slip from the point of transverse anchor  (representing midpoint of two adjacent cracks in a beam) to the loaded end of concrete (representing crack face). The three formulae as expressed in equations 1 to 3 were developed for plain mild steel, cold-worked and hot rolled steel rebars respectively as follows (Kankam, 1997, 2008):

- Plain round bar: fb = (41.7 – 0.2fs) Δ0(8 ……………………. Eq. (1)

- Cold worked bar: fb = (55 – 0.5x) Δ0.5 …………………. …. Eq. (2)

- Hot rolled bar: fb = (35 – 0.3x) Δ0.5 ……………………….... Eq. (3)

where: fb = bond stress (N/mm2); x = distance from center of embedment (mm), fs = steel stress and Δ = total slip of embedded bar. The constant 35 and the coefficient 0.3 are dependent on variables such as bar size, concrete strength, loading type, and surface texture of rebars (Kankam 1997, 2003). The average bond stress calculated was based on choosing two points on the embedded bar. In this paper, however, the formula for hot-rolled steel bars was adopted since the specimens for this study were reinforced with hot-rolled deformed rebars. The formula for hot-rolled steel bars with defined parameters is expressed as in equation 3 above. The average bond stress for the starting point of the embedment (x = x2 = 100mm) and the center (anchored) point of the embedment (x = x1 = 0mm) for a total measured slip of the embedded length is computed using equation 4 which is derived from equation 3:

fb = [(35 - 0.3x1) Δ0.5 + (35 - 0.3x2) Δ0.5]/2 ………………………………Eq. (4)

X1 = 0 (from center of embedment)

X2 = 100 (from center of embedment to face where the rebar enters the specimen [crack face])

Δ = slip (mm)

Fig. 2: Rebar preparation, coating and geometry information processes.

Fig. 3: Bond specimen preparation processes.

Fig. 4: Bond specimen testing setup.

3. Results and Discussion

The local bond stress against slip relationships of the double pull-out test are presented as graphs for the various reinforcing bar types and sizes coated with various coating treatment. Mild steel and high yield steel bars of 12 and 16mm were coated with Gloss, Matt and Red-oxide leyland Laylac oil paint brands, from 1 to 3 coats. These were compared with uncoated (0-coat) rebar counterparts and the differences ascertained statistically with one-way ANOVA. The graphs are presented in figures 5 to 12.

3.1 Influence of the number of coating (1 to 3)

Fig. 5 indicates the effect of number of coats for gloss to 16 mm mild steel bar. There were 18 specimens in all, 6 each for 1, 2 and 3 coats (Fig. 5a-c). Thus, each coating number has 6 specimens compared to that of the uncoated (Fig 5d). The incremental loading was within the service stress limit 140N/mm2 of the rebars. It can be seen that on average the bond stress was 8.5 N/mm2 for all the specimens but they vary on slip characteristics. The specimen with the least slip of 0.104mm was GM16-23T (mild steel, of 2 gloss paint coats) while the largest slip of 0.52mm was GM16-23B (specimen 3 of 2 coats). Majority of the specimens had slip below 0.2mm.

The shape of curves are largely curvilinear but steeper from the starting to about 2.8 N/mm2 bond stress at 0.03 mm slip.  This is an indication that the increase in slip led to gradual increase in the local bond stress, in line with (Mofidi et al., 2024; Wang et al., 2024; Chen et al., 2025; Tang et al., 2025; Fayette et al., 2024; Lee et al., 2025; Tang & Cheng, 2020; Sabău et al., 2016) while a decrease in bond stress led to somewhat rapid slip increase. Similarly, while the tensile loading increased, the bond stress also increased. This shows the specimens were demonstrating about the same characteristics under load.

On the part of 12mm mild steel bar, the average bond stress within the service stress limit was above 12.5N/mm2 while the least slip recorded was 0.09 mm for GM12-23T (3rd specimen of 2 coats of gloss), and the largest bond slip was 1.09 mm for GM12-13B at 20.92N/mm2 (specimen 3 of 1 gloss coat). Most specimens of the multiple coats (2 and 3) had bond slip corresponding with their maximum local bond stress at service load were below 0.22 mm while most specimens of the 1 coat were above 0.22 mm slip, but not more than 0.8mm (Fig. 6). Careful observation of the curves shows that increasing coating led to slight decrease in bond stress for 12mm mild steel bar, but the reverse was the case for the 16mm specimens.

This shows that the higher the coat number, the lower the slip with its corresponding average local bond stress for the 12mm mild steel rebar coated with gloss. The curves appeared steeper from starting up to about 3N/mm2 and then turned curvilinear with uniformly increasing bond stress and slip. The curves are also close to each other on their path. This could be due to the resistance of the pilling of the coat during the tensile pull clogging the path of slip, leading to increasing local bond stress.

Fig. 5 Local bond stress – slip relationship for gloss paint coated 16mm mild steel rebar

| (a) Local bond stress – slip relationship for 1 coat gloss paint to 12mm mild steel rebar. | (b) Local bond stress – slip relationship for 2 coats gloss paint to 12mm mild steel rebar. |
| --- | --- |
| (c): Local bond stress – slip relationship for 3 coats gloss paint to 12mm mild steel rebar. | (d) Local bond stress – slip relationship for 0 - coat paint to 12mm mild steel rebar. |
| Fig. 6: Local bond stress – slip relationship for gloss paint coated 12mm mild steel rebar |  |

3.2 Gloss coated high yield bars

The next category is gloss coated 16mm and 12mm high yield steel bars. The service stress limit corresponds with 250N/mm2. From Fig. 7, the maximum average local bond stress for 16mm is 9 N/mm2 while the least bond slip of 0.092mm at bond stress of 6Nmm2 emanated from GH16-31T (gloss coated 16mm high yield steel, specimen 1 of 3 coats). The maximum slip was 0.40 mm at bond stress of 12.7N/mm2 for GH16-31B. Majority of the 18 specimens produced slip below 0.21mm irrespective of the number of coats. Generally, the curves were linear and steeper with small slip at the start of the tensile load especially the multiple coats, indicating elastic to inelastic behaviour, but became uniformly curvilinear with increasing load. At each loading regime, bond stress and slip of each specimen vary positively. Similar trend can be seen for 12mm high yield steel bar (Fig. 8), but the maximum local bond stress was 18.3N/mm2 for 0.84mm slip, while the least bond slip was 0.133 mm at 7.6N/mm2 bond stress for Gh12-11B and GH12-31T respectively. Majority of the specimens developed slip under 0.3mm and these were largely by 2 and 3 coats specimens. This also indicate reduced bond slip with increasing number of coats especially for the 12mm high yield steel bar. The curves are largely linear and steep from the start but become curvilinear with increased tensile load, accompanied by higher local bond stress, although small in magnitude.

3.3 Matt coats to mild and high yield steel bars

Another set of curves is on the Matt coat to both mild and high yield steel bars. The number of coats as usual was 1 to 3 coat. From Fig. 9, the 16mm mild steel bar coated with Matt shows maximum local bond stress corresponding with the service stress limit as 10.66 N/mm2 at 0.28 mm slip, while the least bond slip of was 0.11 mm at 6.90N/mm2 bond stress for (MM16-11B) and (MM16-31T) respectively. But the specimens, mostly for multiple coats slipped below 0.15 mm while 1 coat specimens slipped more than 0.15 mm nonetheless below 0.284 mm with corresponding greater bond stress. This is another indication that higher coats 2 and 3 resisted bond slip with lower bond stress. This could be due to splitting of the single coat during the tensile pull. The curves did not differ from those previously described. The same trend of characteristics was seen for 12mm mild and high yield steel rebars counterparts, except that their local bond stresses were higher (about 35%) in magnitude, especially for 1-coat specimens (see Fig. 10. 11 and 12). It means that the 12mm mild and high yield steel bars show better bond stress compared to their 16mm counterparts; indicating higher energy absorption capacity as well. This observation aligns with previous studies (Parida and Moharana, 2024; Shunmuga Vembu & Ammasi, 2023; Tunç et al., 2021) though they did not involve coatings. However, Matt coated 16mm high yield rebar did not follow the trend of increased coat leading to decreasing bond stress. It rather showed a clear trend of increasing bond stress and slip with increasing Matt coat. The condition may be due to certain surface characteristics that improved mechanical interlock.

Fig. 7: Local bond stress – slip relationship for gloss paint coated 16mm high yield steel rebar.

| (a): Local bond stress – slip relationship for 1 coat gloss paint to 12mm high yield steel rebar. | (b): Local bond stress – slip relationship for 2 coats gloss paint to 12mm high yield steel rebar. |
| --- | --- |
| (c): Local bond stress – slip relationship for 3 coats gloss paint to 12mm high yield steel rebar. | (d) Local bond stress – slip relationship for 0-coat paint to 12mm high yield steel rebar. |
| Fig. 8: Local bond stress – slip relationship for gloss paint coated 12mm high yield steel rebar. |  |
| (a): Local bond stress – slip relationship for 1 coat matt paint to 16mm mild steel rebar. | (b): Local bond stress – slip relationship for 2 coats matt paint to 16mm mild steel rebar. |
| (c): Local bond stress – slip relationship for 3 coats matt paint to 16mm mild steel rebar. | (d): Local bond stress – slip relationship for 0- coat paint to 16mm mild steel rebar. |
| Fig. 9: Local bond stress – slip relationship for matt paint coated 16mm mild steel rebar |  |

| (a): Local bond stress – slip relationship for 1 coat matt paint to 12mm mild steel rebar. | (b): Local bond stress – slip relationship for 2 coats matt paint to 12mm mild steel rebar. |
| --- | --- |
| (c): Local bond stress – slip relationship for 3 coats matt paint to 12mm mild steel rebar. | (d): Local bond stress – slip relationship for 0 - coat paint to 12mm mild steel rebar. |
| Fig. 10: Local bond stress – slip relationship for matt paint coated 12mm mild steel rebar |  |

| (a): Local bond stress – slip relationship for 1 coat matt paint 16mm high yield steel rebar | (b): Local bond stress – slip relationship for 2 coats matt paint to 16mm high yield steel rebar. |
| --- | --- |
| (c): Local bond stress – slip relationship for 3 coats matt paint to 16mm high yield steel rebar. | (d): Local bond stress – slip relationship for 0-coat paint to 16mm high yield steel rebar. |
| Fig. 11: Local bond stress – slip relationship for matt paint coated 16mm high yield steel rebar. |  |
| (a): Local bond stress – slip relationship for 1 coat matt paint 12mm high yield steel rebar | (b): Local bond stress – slip relationship for 2 coats matt paint to 12mm high yield steel rebar. |
| (c): Local bond stress – slip relationship for 3 coats matt paint to 12mm high yield steel rebar. | (d): Local bond stress – slip relationship for 0-coat paint to 12mm high yield steel rebar. |
| Fig. 12: Local bond stress – slip relationship for matt paint coated 12mm high yield steel rebar. |  |

3.4	Red oxide coat in mild and high yield bars

The 3rd brand of paints used was red-oxide and the results on both 16 mm and 12 mm mild and high yield steel reinforcing bars as presented in figures 13-16. They also followed the trend of increasing coating leading to decreasing local bond stress/strength across the board. All the characteristics followed the earlier coating conditions. The 12mm mild and high yield rebars show higher local bond stress values, about 29% above their 16mm counterparts. For example, Fig. 13 shows maximum local bond stress of 17.98 N/mm2 at 0.81mm slip and, the least slip of 0.11mm at 6.64N/mm2 local bond stress for RM16-23B and RM16-33T respectively. Also Fig. 14 indicates 21.95N/mm2 as highest local bond stress at 1.20mm slip from RM12-12T. Similarly, figures 15 and 16 indicate maximum local bond stress of 10.38N/mm2 at 0.27 bond slip and least bond stress of 7.42 N/mm2 at 0.14 mm bond slip for RH16-11B and RH16-33T respectively; while maximum local bond stress of 17.40N/mm2 at 0.76mm bond slip, and the least bond of 8.50N/mm2 at 0.18mm bond slip for RH12-13T and RH12-23T respectively. The variation between the slip of the various specimens could be due to the fact that compaction quality might vary. But it could be observed that with red-oxide effect, mild steel rebars show better performance on bond than the high yield counterparts.

| (a): Local bond stress – slip relationship for 1 coat red-oxide paint to 16mm mild steel rebar. | (b): Local bond stress – slip relationship for 2 coats red-oxide paint to 16mm mild steel rebar. |  |
| --- | --- | --- |
| (c): Local bond stress – slip relationship for 3 coats red-oxide paint to 16mm mild steel rebar. | (d): Local bond stress – slip relationship for 0- coat paint to 16mm mild steel rebar. |  |
| Fig. 13: Local bond stress – slip relationship for red-oxide paint coated 16mm mild steel rebar |  |  |
| (a): Local bond stress – slip relationship for 1 coat red-oxide paint to 12mm mild steel rebar. |  | (b): Local bond stress – slip relationship for 2 coats red-oxide paint to 12mm mild steel rebar. |
| (c): Local bond stress – slip relationship for 3 coats red-oxide paint to 12mm mild steel rebar. |  | (d): Local bond stress – slip relationship for 0 - coat paint to 12mm mild steel rebar. |
| Fig. 14: Local bond stress – slip relationship for red-oxide paint coated 12mm mild steel rebar |  |  |
| (a): Local bond stress – slip relationship for 1 coat red-oxide paint 16mm high yield steel rebar | (b): Local bond stress – slip relationship for 2 coats red-oxide paint to 16mm high yield steel rebar. |  |
| (c): Local bond stress – slip relationship for 3 coats red-oxide paint to 16mm high yield steel rebar. | (d): Local bond stress – slip relationship for 0-coat paint to 16mm high yield steel rebar. |  |
| Fig. 15: Local bond stress – slip relationship for red-oxide paint coated 16mm high yield steel rebar. |  |  |

| (a): Local bond stress – slip relationship for 1 coat red-oxide paint 12mm high yield steel rebar | (b): Local bond stress – slip relationship for 2 coats red-oxide paint to 12mm high yield steel rebar. |
| --- | --- |
| (c): Local bond stress – slip relationship for 3 coats red-oxide paint to 12mm high yield steel rebar. | (d): Impact of coating number on local bond stress – slip relationship for red-oxide paint to 12mm high yield steel rebar. |
| Fig. 16: Local bond stress – slip relationship for red-oxide paint coated 12mm high yield steel rebar. |  |

3.4	Control specimens with uncoated bars

In order to give a fair judgment of the performance of the coatings on bond and slip, the bond stress - slip curve were also presented for the control specimens. Fig. 17 shows both mild and high yield steel rebars. It indicates that uncoated mild and high yield reinforced concrete prism specimens curve shape characteristics are not different from the coated rebars discussed above. Careful observation shows that the curvilinear shape starts about 3 N/mm2 bond stress for most of the specimens. The maximum local bond stress estimated corresponding with the service stress limit was 9.09 N/mm2 at 0.21 mm slip from CM16-3T. The least local bond was 7.62 N/mm2 at 0.14 mm slip for CM16-1B. Similarly, the 12 mm uncoated mild steel bar exhibited maximum bond stress of 8.34 N/mm2 at 0.18mm slip and the least bond was 7.08N/mm2 at 0.13mm slip for CM12-1B and CM12-3T respectively. Also, 16mm high yield steel rebar show maximum bond stress of 19.07 N/mm2 at 0.91mm slip while the least bond was 10.15N/mm2 at 0.26mm bond slip for CH16-1T and CH16-2B respectively. The specimens with 12mm bar had maximum local bond stress of 13.20 N/mm2 at 0.44mm slip, with least local bond stress 8.35N/mm2 at 0.17mm slip for CH12-2B and CH12-1T respectively.

It could be observed from the foregoing that the uncoated 16 mm rebars show higher local bond stress (about 24%) compared to 12mm uncoated rebars, contrary to established findings that smaller diameter bars develop greater anchorage bond stress than larger bars (Parida and Moharana, 2024; Shunmuga Vembu & Ammasi, 2023; Tunç et al., 2021). But the reverse was the case for all coated rebars irrespective of paint types or number of coats. The average variations in local bond and bond slip in each case was ascertained for significance difference statistically with the aid of one-way analysis of variance (ANOVA).

| (a): Local bond stress – slip relationship for uncoated 16mm mild steel rebar | (b): Local bond stress – slip relationship for uncoated 12mm mild steel rebar. |
| --- | --- |
| (c): Local bond stress – slip relationship for uncoated 16mm high yield steel rebar. | (d): Local bond stress – slip relationship for uncoated 12mm high yield steel rebar. |
| Fig. 17: Local bond stress – slip relationship for uncoated mild and high yield steel rebars. |  |

3.6	Impact of paint coating type on local bond and slip.

This section discusses whether the type of paint brand (viz, gloss, matt, red-oxide) affects bond and slip. Fig. 18 illustrates the result of the specimens from the selected paints and uncoated specimens of mild steel. The curves show no varied difference in shape, but it can be seen that all the coated specimens show better bond than the uncoated. While the curves of the uncoated specimens fall under 9N/mm2 bond, the coated (gloss, matt and red-oxide) fall beyond 9N/mm2. This trend for result of 12mm coated mild steel rebar remains the same for 16mm mild steel as seen in Fig. 19. The red-oxide coated specimen shows better local bond over gloss, matt and uncoated in that order. This shows the local bond potency of the coats on mild steel rebar. This is contrary to earlier findings where epoxy coating reduced bond by at least 10% (Kayali and Yeomans, 2000; Shunmuga Vembu & Ammasi, 2023). Thus, the selected paints in this study are superior to epoxy but rank apar with galvanized steel rebar.

Similarly, Fig. 20 shows 12mm high yield steel rebars coated with the various paints. The coated specimens’ curves show better local bond over the uncoated specimens. Individually the performance of all the paint types were at par on local bond strength. All the coated specimens have some specimens above 15N/mm2 but the uncoated was below 14N/mm2. Hence, with the 12mm high yield steel rebar, the coated specimens performed better than the uncoated but this does not vary with the paint type. However, in the case of 16mm high yield steel rebar, the uncoated rebar was better on local bond strength than the coated rebar specimens as seen in Fig 21; supporting Shunmuga Vembu & Ammasi, 2023. Also, the gloss and matt paint coats show better local bond strength over red-oxide, which is the direct opposite situation of the coated 16mm mild steel rebar counterpart. While some of the 16mm uncoated high yield steel rebar specimens hit above 14N/mm2, local bond Strength for all 16mm coated high yield steel rebar specimens hit below 14N/mm2. The surface features and other features like compaction and curing quality differences could be the result of the variations seen.

| (a): Impact of coating type on local bond stress – slip relationship for gloss paint to 12mm mild steel rebar. | (b): Impact of coating type on local bond stress – slip relationship for matt paint to 12mm mild steel rebar. |
| --- | --- |
| (c): Impact of coating type on local bond stress – slip relationship for red-oxide paint to 12mm mild steel rebar. | (d): Impact of coating type on local bond stress – slip relationship for uncoated 12mm high yield steel rebar. |
| Fig. 18: Rebar coating type and local bond stress – slip relationship for paint coated mild and steel rebars. |  |

| (a): Impact of coating type on local bond stress – slip relationship for gloss paint to 16mm mild steel rebar. | (b): Impact of coating type on local bond stress – slip relationship for mat paint to 16mm mild steel rebar. |
| --- | --- |
| (c): Impact of coating type on local bond stress – slip relationship for red-oxide paint to 16mm mild steel rebar. | (d): Impact of coating type on local bond stress – slip relationship for zero paint to 16mm mild steel rebar. |
| Fig. 19: Rebar coating type and local bond stress – slip relationship for paint coated mild and steel rebars. |  |

| (a): Impact of coating type on local bond stress – slip relationship for gloss paint to 12mm mild steel rebar. | (b): Impact of coating type on local bond stress – slip relationship for matt paint to 12mm mild steel rebar. |
| --- | --- |
| (c): Impact of coating type on local bond stress – slip relationship for red-oxide paint to 12mm high yield steel rebar. | (d): Impact of coating type on local bond stress – slip relationship for zero paint to 12mm high yield steel rebar. |
| Fig. 20: Rebar coating type and local bond stress – slip relationship for paint coated high yield steel rebars. |  |

| (a): Impact of coating type on local bond stress – slip relationship for gloss paint to 16mm mild steel rebar. | (b): Impact of coating type on local bond stress – slip relationship for matt paint to 16mm mild steel rebar. |
| --- | --- |
| (c): Impact of coating type on local bond stress – slip relationship for red-oxide paint to 16mm high yield steel rebar. | (d): Impact of coating type on local bond stress – slip relationship for zero paint to 16mm high yield steel rebar. |
| Fig. 21: Rebar coating type and local bond stress – slip relationship for paint coated high yield steel rebars. |  |

4.0	Observation on bond specimens

Under low applied tension axial with relatively elastic characterization, the rebar diameter reduces in a minute to macro loss in bond while promoting shear. Hence, as the rebar slipped with shear, the bond tended to increase again, which might be due to clogging of sheared concrete, paint in the rib spaces resisting slip. In a few cases where there was a specimen failure during the pull, the concrete split vertically in the direction of the tensile pull towards the center of the specimen. The crack also started from the pulling side where the rebar was in contact with the concrete. In a few cases where it was tested to failure, there was sign of shear concrete stack in the corner of the ribs or within the rib spaces. There was some sign of micro pealing of the coating stain sticking to the concrete. This shows how the coated rebars bonded with the concrete. The behaviour was not different from that of the uncoated rebars. It also shows that at a strong pull which is beyond the bond strength between the coated rebar and the concrete, the coats if not properly cured could pill easily. The sign of coat sticking to concrete seen could also be due to reaction between the concrete and the paint coat. See pictures in Fig. 22.

Fig. 22: Bond failure observation in prism double pull-out test.

Statistical Analysis of Local Bond strength and Slip

The above discussed results relied on facial judgment on parameter/variable based on the bond – slip graphs. Hence the one-way ANOVA was run on the data to confirm or dispute the outcome, in order that cause and effect could be attributed. The first considers influence of the paint coat - gloss, mat and red-oxide as against no paint coating on local bond. The results are captured in Tables 2-8 and figures 23 - 25.

Table 2a: Mean and standard deviation of local bond strength for paint type on rebar

| Group | N | Mean | Sd |
| --- | --- | --- | --- |
| No-Paint | 24 | 10.07 | 2.92 |
| Red-oxide | 72 | 10.64 | 3.09 |
| Matt | 72 | 9.61 | 2.70 |
| Gloss | 72 | 10.00 | 3.21 |
| Total | 240 | 10.08 | 3.01 |

Source: Lab result 2024      sd = standard deviation

From Table 2a, the means of values derived from local bond stress test for the various paint type coat to reinforcing steel bars are presented. The local bond strength for red-oxide, No-Paint, gloss and matt paint coats are shown. The values vary, but look close in magnitude. Thus, M(72) = 10.64 > M(24) = 10.07 > M(72) = 10.00 > 9.61 respectively. Table 1b ascertains whether the differences between the means are significant or not.

Table 2b: One-way ANOVA summary of local bond strength for paint types on rebar

| Group | Sum of squares | df | Mean square | F | p-value | p |
| --- | --- | --- | --- | --- | --- | --- |
| Between Groups | 38.80 | 3 | 12.93 | 1.44 | 0 .23 | >0.05 |
| Within Groups | 2125.37 | 236 | 9.01 |  |  |  |
| Total | 2164.18 | 239 |  |  |  |  |

Source: Lab result 2024

As shown in Table 2b, the result F (3, 239) = 1.44, P > 0.05 indicates that no significant difference exists between at least two of the means of the paint coated reinforcing steel bars and the control specimens tested on local bond strength, at 0.05 level of significance. Nonetheless, it can be seen from the post hoc analysis in Table 2c that the mean difference in values Md = - 0.57, P > 0.05

Table 2c: Post hoc summary of local bond strength for paint types steel bar

| Paint Type | 1 | 2 | 3 | 4 |
| --- | --- | --- | --- | --- |
| No Paint |  |  |  |  |
| Red-oxide | - 0.57 |  |  |  |
| Mat | 0.46 | 1.03 |  |  |
| Gloss | 0.07 | 0.64 | - 0.39 |  |

Source: Lab result 2024		       * means significant at 0.05

between coated rebars (red-oxide) and the control or uncoated rebars and other coated rebars indicate generally no significant difference in local bond strength within coated and between uncoated specimens at 0.05 level of significance. Therefore, the differences seen between the means could be due to chance. Hence, they were about the same in local bond strength whether coated or not, and the assumption that variation might exist between the local bond strength of coated and uncoated rebars used in the study was not confirmed. See Fig. 23a for the graphical presentation. This did not support (Treece and Jirsa, 1989; Shunmuga Vembu & Ammasi, 2023) in the case of epoxy coated. It means that the selected coating materials used in the current study have special features that promoted bonding effect.

Fig. 23a: Average local bond strength for paint types			Fig. 23b:  Average local slip for paint types

Table 3a: Mean and standard deviation of slip for paint type on rebar

| Group | N | Mean | Sd |
| --- | --- | --- | --- |
| No Paint | 24 | 0.27 | 0.18 |
| Red-oxide | 72 | 0.31 | 0.20 |
| Mat | 72 | 0.25 | 0.15 |
| Gloss | 72 | 0.27 | 0.20 |
| Total | 240 | 0.28 | 0.18 |

Source: Lab result 2024

From Table 3a, the statistical means for the various paint types vary superficially in face value for slip within concrete. Thus, M(72) = 0.31 > M(72) = 0.27 = M(24) = 0.27 > M(72) = 0.25, for Red-oxide, Gloss, No-Paint (Control) and Mat paints respectively. Ascertaining whether these differences were not due to chance, the one-way ANOVA analysis in   Table 3b is presented for the discussion.

Table 3b: One-way ANOVA summary of slip for paint type on steel bar

| Group | Sum of squares | df | Mean square | F | p-value | p |
| --- | --- | --- | --- | --- | --- | --- |
| Between Groups | 0.12 | 3 | 0.04 | 1.23 | 0.3 | >0.05 |
| Within Groups | 7.91 | 236 | 0.03 |  |  |  |
| Total | 8.03 | 239 |  |  |  |  |

Source: Lab result 2024

The result F (3, 239) = 1.23, P > 0.05 from Table 3b indicates that no significant difference exists between at least two of the means of the paint types used and the control on slip at 0.05 level of significance. The post hoc analysis presented in Table 3c identifies the degree of the differences facially seen.

Table 3c: Post hoc summary of slip for paint type on steel bar

| Paint Type | 1 | 2 | 3 | 4 |
| --- | --- | --- | --- | --- |
| No Paint |  |  |  |  |
| Red-oxide | - 0.03 |  |  |  |
| Mat | 0.03 | 0.06 |  |  |
| Gloss | - 0.001 | 0.03 | - 0.03 |  |

Source: Lab result 2024		       * means significant at 0.05

From the post hoc results in Table 3c, the mean differences, Md = -0.03, P > 0.05; Md = 0.03, P > 0.05 and Md = -0.001, P > 0.05 confirms that there is no significant difference between the mean of slip for No paint, Red-oxide, Mat and Gloss paints used at 0.05 level of significance. Therefore, the differences seen between their means were due to chance. Hence, they were about the same level of retarding slip within the concrete. This defeats the assumption that variation may exist in the slip retarding capacity of paint coated and uncoated rebars in concrete. The value 0.03 shows matt brand of the paints performed better in local slip retardation than the uncoated rebar, red-oxide and gloss paint coated rebars; followed by uncoated, gloss and red-oxide in that order; except that the differences were not significant. This shows that the paints used in the study have the capacity to retard bond slip within concrete when coated to rebars up to three coats for corrosion protection.   The mean plot for the slip between concrete and rebar whether coated or uncoated is also presented in Fig. 23b for further clarification graphically.

The above did not consider the number of coats of protection to rebars. Table 4 and 5 concentrated on specifics to determine the effect of number of coats to rebar on local bond stress and slip.

Table 4a: Mean and standard deviation of local bond strength for number of paint coats to rebar

| Group | N | Mean | Sd |
| --- | --- | --- | --- |
| Zero-coat | 24 | 10.07 | 2.92 |
| One-coat | 72 | 11.86 | 3.50 |
| Two-coats | 72 | 9.18 | 2.57 |
| Three-coats | 72 | 9.21 | 2.00 |
| Total | 240 | 10.01 | 3.01 |

Source: Lab result 2024

From Table 4a and Fig.24a, the means values of local bond stresses for the various number of coats and uncoated rebars are presented. It shows that the two-coat rebar had the least bond stress of M(72) = 9.18 < M(72) = 9.21 = M(24) = 10.07 = M(72) = 11.86, for two, three, zero and one coat respectively. This means that one paint coat shows higher local bond stress over zero and other coats. However, in order to ascertain whether the difference in local bond stress between the number of coats, the one-way ANOVA result from Table 3b is next presented for consideration.

Table 4b: One-way ANOVA summary of local bond strength for number of paint coat to rebar

| Group | Sum of squares | df | Mean square | F | p-value | p |
| --- | --- | --- | --- | --- | --- | --- |
| Between Groups | 341.78 | 3 | 113.93 | 14.75 | 0.00 | <0.05 |
| Within Groups | 1822.40 | 236 | 7.72 |  |  |  |
| Total | 2164.18 | 239 |  |  |  |  |

Source: Lab result 2024

The result F (3, 239) = 14.75, P < 0.05 from Table 4b indicates that significant difference exists between at least two of the means of the number of coats to the reinforcing steel bar on local bond at 0.05 level of significance. The post hoc analysis shows areas of existence of the difference in the result between the numbers of coats in Table 4c.

Table 4c: Post hoc summary of local bond strength for number of paint coats to rebar

| Number of coat | 1 | 2 | 3 | 4 |
| --- | --- | --- | --- | --- |
| Zero-coat |  |  |  |  |
| One-coat | -1.79* |  |  |  |
| Two-coat | 0.89 | 2.68* |  |  |
| Three-coat | 0.86 | 2.65* | -0.03 |  |

Source: Lab result 2024		       * means significant at 0.05

From the post hoc results in Table 4c, the mean differences Md = -1.79, P < 0.05; shows that there is significant difference at 0.05 level of significance between the uncoated rebar and one-coat rebar specimens in favour of one-coat rebar; but no significant difference exists between two-coats and three-coats and zero (uncoated) rebar specimens as per Md = 0.89, P > 0.05 and Md = 0.86, P > 0.05 respectively. Similarly, Md = 2.68, P < 0.05 and Md = 2.65, P < 0.05 for two-coat and three-coat show that one-coat was superior in bond stress than two and three coats specimens at 0.05 level of significance. However, Md = -0.03, P > 0.05 indicates that no significance difference exists between two-coat and three-coat specimens on bond stress performance. Though the number of coats affects bond stress (Charles et al. (2018); Shunmuga Vembu & Ammasi, 2023; Yuanliang et al., 2016), cumulatively, looking at the specifics in terms of number of coats, all levels of paint coat show better or slightly about the same local bond stress in concrete compared to the uncoated rebars. This indicates that each number of paint coatings used in the study has the capacity to retard local bond stress depletion between concrete when used to protect rebar against corrosion (see Fig. 24a).

Fig. 24a: Local bond strength plot for number of paint coating	   Fig.24b: Local slip plot for number of paint coating

The next analysis looks at the effect of coating levels on the corresponding slip between concrete and coated rebars. Table 5a presents the means and standard deviation of the bond slip for the various levels of coating – zero, one, two and three coats.

Table 5a: Mean and standard deviation of slip for number of paint coats to rebar

| Group | N | Mean | Sd |
| --- | --- | --- | --- |
| Zero-coat | 24 | 0.27 | 0.18 |
| One-coat | 72 | 0.38 | 0.23 |
| Two-coats | 72 | 0.23 | 0.14 |
| Three-coats | 72 | 0.22 | 0.10 |
| Total | 240 | 0.28 | 0.18 |

Source: Lab result 2024

From Table 5a and Fig.24b, the means for the various number of coats vary superficially in slip value with the one coat showing the higher local slip followed by the uncoated steel bar. Thus M(72) = 0.380 > M(24) = 0.274 > M(72) = 0.227 > M(72) = 0.222, respectively for one–coat, zero-coat, two-coats and three-coats. However, in order to ascertain whether these differences are not due to chance, the one-way ANOVA result from Table 5b is next presented for consideration.

Table 5b: One-way ANOVA summary of slip for number of paint coats to rebar

| Group | Sum of squares | df | Mean square | F | p-value | p |
| --- | --- | --- | --- | --- | --- | --- |
| Between Groups | 1.17 | 3 | 0.39 | 13.39 | 0.00 | <0.05 |
| Within Groups | 6.86 | 236 | 0.03 |  |  |  |
| Total | 8.03 | 239 |  |  |  |  |

Source: Lab result 2024

The result F (3, 239) = 13.39, P < 0.05 from Table 5b indicates that significant difference exists between at least two of the means of the number of coats to the reinforcing steel bar on local slip within concrete at 0.05 level of significance. Post hoc analysis in Table 5c identifies the variables that shows the significant difference in slip.

Table 5c: Post hoc summary of bond slip for number of paint coats to rebar

| Number of coat | 1 | 2 | 3 | 4 |
| --- | --- | --- | --- | --- |
| zero-coat |  |  |  |  |
| One-coat | -0.11* |  |  |  |
| Two-coats | 0.05 | 0.15* |  |  |
| Three-coats | 0.05 | 0.16* | 0.005 |  |

Source: Lab result 2024		       * means significant at 0.05

From Table 5c, the mean differences Md = -0.11, P < 0.05; shows there is significant difference between the slip of zero-coat and one-coat, where one-coat displayed more slip than the zero-coat reinforcing steel bar, in line with Yuanliang et al. (2016). Similarly, Md = 0.15, P < 0.05 and Md = 0.16, P < 0.05 indicate that there is significant difference at 0.05 level of significance between the mean slip of one-coat and two-coats and three-coats. The positive difference means one-coat produced higher slip than two-coats and three-coats protected rebars. This is because the local bond increased with increased slip. On the other hand, Md = 0.05, P > 0.05; Md = 0.05, P > 0.05 ascertained that there were no significant differences between means for zero-coat, two-coat and three-coat rebars at 0.05 level of significance. Rather, the slight positive differences seen, though due to chance, were in favour of zero-coat as can be seen from Fig. 24b.  This means that zero-coat, two-coat and three-coat show better resistance to local slip within concrete compared to one-coat. The facial outlook from the graph portrayed three-coat to be the best in local slip resistance. The outcome hinges on the better local bond stress displayed over the uncoated rebars in concrete. Hence, the assumption that variation might exist between coated and uncoated rebars in their slip resistance was confirmed. Thus, either two-coat or three-coat of the paints used in the study has very high (more than 19%) local slip resistance over the uncoated rebar. This may be due to the cushion provided by the thickness of the film interlocking with sand particles or clogging, and thereby increasing resistance to local slip while promoting the local bond stress. This supports the trend shown by the bond-slip graphs on number of coating, where largely increased coat saw decreased local bond (Shunmuga Vembu & Ammasi, 2023; Yuanliang et al., 2016).

The study also considered the type of steel bar coated – mild and high yield steel bars - to examine its effect on bond stress and slip. Tables 6a and 6b present the outcome of the results.

Table 6a: Mean and standard deviation of local bond for coated steel type

| Group | N | Mean | Sd |
| --- | --- | --- | --- |
| Mild Steel | 108 | 9.86 | 3.24 |
| High Yield steel | 108 | 10.30 | 2.67 |
| Total | 216 | 10.08 | 3.03 |

Source: Lab result 2024

Table 6a, presents the means for mild and high yield steel bars coated for the experiment. It can be seen that the mean value of high yield steel bar is slightly greater than that of mild steel bar. Thus, M(108) = 10.30 > M(108) = 9.86. The significance of the difference seen is ascertained by one-way ANOVA result from Table 6b.

Table 6b: One-way ANOVA summary of local bond for coated steel type

| Group | Sum of squares | df | Mean square | F | p-value | p |
| --- | --- | --- | --- | --- | --- | --- |
| Between Groups | 10.39 | 1 | 10.39 | 1.14 | 0.27 | >0.05 |
| Within Groups | 1957.23 | 214 | 9.15 |  |  |  |
| Total | 1967.63 | 215 |  |  |  |  |

Source: Lab result 2024

From Table 6b, the result F (1, 215) = 1.14, P > 0.05, indicates that no significant difference exists between local bond stress of coated high yield reinforcing steel bars and coated mild steel bars at 0.05 level of significance. It shows that the local bond stress of coated high yield steel bar was about the same for mild steel rebar. This may be due to enhance physical properties due to the coating film reducing the effect of the sharp edges of the ribs of the rebars, and thereby reducing the ability of the edge to scratch the surface of the concrete during the pull. The corresponding local slip behaviour also shows no significant difference, due to the positive relation trend of local bond and slip.

However, when the control (uncoated) rebar counterparts were tested, it proved otherwise. Tables 6c and d present the results as follows.

Table 6c: Mean and standard deviation of local bond for uncoated steel type

| Group | N | Mean | Sd |
| --- | --- | --- | --- |
| Mild Steel | 12 | 7.96 | 0.66 |
| High Yield steel | 12 | 12.19 | 2.77 |
| Total | 24 | 10.07 | 2.92 |

Source: Lab result 2024

Table 6c, presents the means for uncoated mild and high yield steel bars. It can be seen that the mean value of high yield steel is almost twice that of mild steel. Thus, M(12) = 12.19 > M(12) = 7.96. The difference seen is ascertained by one-way ANOVA result from Table 6d,

Table 6d: One-way ANOVA summary of local bond for uncoated steel type

| Group | Sum of squares | df | Mean square | F | p-value | p |
| --- | --- | --- | --- | --- | --- | --- |
| Between Groups | 107.56 | 1 | 107.56 | 26.59 | 0.00 | <0.05 |
| Within Groups | 88.99 | 22 | 4.05 |  |  |  |
| Total | 196.55 | 23 |  |  |  |  |

Source: Lab result 2024

From Table 6d, the result F (1, 23) = 26.59, P < 0.05, indicates that a significant difference exists between local bond stress of uncoated high yield reinforcing steel bar and uncoated mild steel bar at 0.05 level of significance. It shows that the local bond stress of uncoated high yield steel bar was higher and better than that of uncoated mild steel bar. This may be due to the better physical properties, such as rib height and spacing that aided a better mechanical interlock (Biney et al., 2024). The corresponding slip equally showed significant difference between high yield and mild steer rebars following the local bond. Hence, it can be said that the coating had effect on the rebar types used, by improving the local bond of the mild steel bar to match with the local bond of high yield bar.

The next is to determine the effect of various reinforcing steel bar sizes and type on local bond and slip. Tables 7 and 8 as well as Fig. 25 present the outcome as follows.

Table 7a: Mean and standard deviation of local bond strength for coated steel bar size

| Group | N | Mean | Sd |
| --- | --- | --- | --- |
| R12 | 54 | 10.58 | 3.99 |
| R16 | 54 | 9.15 | 2.36 |
| Y12 | 54 | 11.66 | 2.91 |
| Y16 | 54 | 8.94 | 1.45 |
| Total | 216 | 10.08 | 3.03 |

Source: Lab result 2024      R= mild steel   Y = high yield steel

From Table 7a and Fig. 25a, the means for the various steel sizes of coated rebars for the bond test are presented. It can be seen that the mean values vary on bond stress, with Y12 showing the highest bond stress. Thus, M(54) = 11.66 > M(54) = 10.58 > M(54) = 9.15 > M(54) = 8.94, for Y12, R12, R16, and Y16 respectively. The graphical presentation of the trend can be seen from Fig. 25a. These differences were analyzed with one-way ANOVA for significance check as portrayed in Table 7b.

Table 7b: One-way ANOVA summary of local bond strength for coated steel bar size

| Group | Sum of squares | df | Mean square | F | p-value | p |
| --- | --- | --- | --- | --- | --- | --- |
| Between Groups | 266.30 | 3 | 88.77 | 11.06 | 0.00 | <0.05 |
| Within Groups | 1701.32 | 212 | 8.03 |  |  |  |
| Total | 1967.63 | 215 |  |  |  |  |

Source: Lab result 2024

The result F (3, 215) = 11.06, P < 0.05 from Table 7b indicates that a significant difference exists in the local bond stresses between at least two of the means of the sizes of the coated reinforcing steel bars used in the study at 0.05 level of significant. Post hoc analysis in Table 7c identifies the degree of the difference that exists between the local bond stresses of various rebar sizes.

Table 7c: Post hoc summary of local bond strength for coated steel bar size

| Steel Size | 1 | 2 | 3 | 4 |
| --- | --- | --- | --- | --- |
| R12 |  |  |  |  |
| R16 | 1.44* |  |  |  |
| Y12 | -1.08* | -2.52* |  |  |
| Y16 | 1.64* | 0.20 | 2.72* |  |

Source: Lab result 2024		       * means significant at 0.05

From Table 7c, the mean differences Md = 1.44, P < 0.05; Md = -1.08, P < 0.05 and Md = 1.64, P < 0.05 shows that there is significant difference at 0.05 level of significance between the means of R12, and, R16, Y12 and Y16 in that order. It implies that the difference seen between the means of the local bond stresses for the various coated rebar sizes was not due to chance. Again, the result Md = -2.52*, and -2.72* indicated a significant difference between the local bond of coated R16, and, Y12 and Y16 respectively, but not between R16 and Y16 at 0.05 level of significance. This result shows the local bond stress capacity of Y12 and R12 rebars were better than R16 and Y16 though Y12 performed better compared to R12. The current result therefore follows earlier studies that found that the smaller the size of the rebar the better bond stress (Tang & Cheng, 2020; Burdziński & Niedostatkiewicz, 2022; Shunmuga Vembu & Ammasi, 2023). This means that attributes   of the surface area coated did not change the existing trend on bond properties of uncoated rebar. The corresponding slip behaviour between concrete and the coated rebars by their sizes is next.

Fig. 25a: Local bond strength plot for bar sizes coated	       Fig. 25b: Local slip plot for steel bar sizes coated

Table 8a: Mean and standard deviation of slip for coated steel bar sizes

| Group | N | Mean | Sd |
| --- | --- | --- | --- |
| R12 | 54 | 0.32 | 0.25 |
| R16 | 54 | 0.22 | 0.13 |
| Y12 | 54 | 0.36 | 0.19 |
| Y16 | 54 | 0.20 | 0.07 |
| Total | 216 | 0.28 | 0.18 |

Source: Lab result 2024

From Table 8a and Fig. 25b, the means for slip of various sizes and types of rebar up to three coats. The means M(54) = 0.36 > M(54) = 0.32 > M(54) = 0.22 > M(54) = 0.20, are respectively slip for Y12, R12, R16 and Y16 rebars. This is also displayed graphically in Fig. 25b. The one-way ANOVA result from Table 8b informs if the differences were significant.

Table 8b: One-way ANOVA summary of slip for coated steel bar size

| Group | Sum of squares | df | Mean square | F | p-value | p |
| --- | --- | --- | --- | --- | --- | --- |
| Between Groups | 0.90 | 3 | 0.30 | 9.99 | 0.00 | <0.05 |
| Within Groups | 6.39 | 212 | 0.03 |  |  |  |
| Total | 7.30 | 215 |  |  |  |  |

Source: Lab result 2024

The result F (3, 215) = 9.99, P < 0.05 from Table 8b indicates that a significant difference exists between at least two of the means of the local slip of the coated rebars by their various sizes and types at 0.05 level of significance. Post hoc analysis in Table 8c isolates where significant difference occurred between the various sizes.

Table 8c: Post hoc summary of slip for coated steel bar sizes

| Steel Size | 1 | 2 | 3 | 4 |
| --- | --- | --- | --- | --- |
| R12 |  |  |  |  |
| R16 | 0.09* |  |  |  |
| Y12 | - 0.04 | -0.14* |  |  |
| Y16 | 0.11* | 0.02 | 0.16* |  |

Source: Lab result 2024		       * means significant at 0.05

From Table 8c, the mean differences Md = -0.09, P < 0.05; and Md = 0.11, P < 0.05 show that the slip difference seen between R12 and R16 and Y16 respectively, is significant at 0.05 level of significance. Similarly, the result Md = -014* and 0.16* indicated a significant difference between the bond slip of R16 and Y12, and, Y12 and Y16 respectively at 0.05 level of significance, all in favour of Y12. It shows that the differences seen between the means of the slip for the various coated rebar sizes were not due to chance.  But Md = -0.04 > 0.05; and Md = -0.02 > 0.05 indicated that the bond slip differences between R12 and Y12; and, R16 and Y16 were not significant at 0.05 level of significance. Hence, the differences seen were due to chance. It corresponds to the trend of local bond stress of the various coated rebar sizes discussed above, except that R12 and Y12 did not differ on slip significantly.

Conclusion

Double pull-out test was conducted on coated rebar reinforced prism to determine effect of the coat on local bond strength with a view to ascertain its quality in service. The coating involved use of selected local Ghanaian oil paints from Leyland – Gloss, Matt and Red-oxide – to protect rebars against corrosion (Akortia et al., 2024). Number of coat, rebar type and sizes were varied as well to determine their effect on both the coat and the bond. The summarized outcome is as follows:

- The paint coat to the reinforcing steel bars improved local bond and slip in the same quality as the uncoated rebars for all the selected paint brand use in this study. Thus, no significant difference exist between coat and uncoated rebar on local bond stress and lip.

- Increase in number of paint coat saw decrease in local bond strength/stress with corresponding reduction in bond slip. One-coat of paints in this study showed significantly better (18%) bonding quality over zero-coat while two-coat and three-coat were at par with zero-coat.

- No significant difference exist between local bond and slip of mild and high yield steel bars due to the coating. It rather improved their local bond strength.

- The coat improved significantly, the local bond and slip for smaller diameter rebars over the higher diameter rebars for all the rear types. While 12mm high yield showed better local bond over 11N/mm2 with 0.35mm slip than all the other sizes and types of rebars used, 16mm mild steel bar shows the least bond of 9N/mm2 with 0.22mm slip.

- The local bond values of the coated rebars ranged on average from 9N/mm2 to 11N/mm2 across the various rebar sizes and type used in this study. This is comparably better than other earlier studies that did not coat. Kankam (1997) found bond stress of 6.0 - 6.7Nmm2 for ribbed high yield steel bars with higher concrete strength.

- Hence, the selected paints can be applied to reinforcing bar against corrosion in concrete to enhance the integrity and safety of concrete structural elements. The selected paints are therefore recommended to be used as corrosion protection for reinforcing steel bars in concrete structures (under service load) like bridges, coastal building, and water reservoirs among others. Nonetheless the coating thickness must not beyond 220µm.

DISCLAIMER (ARTIFICIAL INTELLIGENCE)

Author(s) hereby declared that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc.) and text-to-image generators have been used during the writing or editing of this manuscript.

COMPETING INTERESTS

There are no known competing financial interests or non-financial interests or personal relationships that could have appeared to influence the work reported in this paper.

References

Akortia, V. K., Kankam, C. K., Biney, E., Dzikunu, P., Afrifa, R. O., & Banahene, J. O. (2024). Assessment of Oil Paints for Corrosion Protection of Reinforcing Steel Bars in Concrete. Journal of Scientific Research and Reports, 30(11), 699–717.https://doi.org/10.9734/jsrr/2024/v30i112598

Biney, E., Kankam, C. K., Akortia, V. K., Adzakey, P., Junior, J. K. Q., & Tongyem, E. (2024). Examining the Geometrical Properties, Chemical Composition, and Mechanical Properties of Local Reinforcing Bars in Ghana. Journal of Engineering Research and Reports, 26(6), 223–240. https://doi.org/10.9734/jerr/2024/v26i61176

Auyeung, Y., Balaguru, P., & Chung, L. (2000). Bond behavior of corroded reinforcement bars. Materials Journal, 97(2), 214–220. https://doi.org/10.14359/826

Parida, L., & Moharana, S. (2024). Mechanical and corrosion investigations of bond behavior in reinforced concrete with varying parameters. Journal of Failure Analysis and Prevention, 24, 402–413. https://doi.org/10.1007/s11668-023-01850-1

Shunmuga Vembu, P. R., & Ammasi, A. K. (2023). A comprehensive review on the factors affecting bond strength in concrete. Buildings, 13(3), 577. https://doi.org/10.3390/buildings13030577

Kankam C.K. (2003). A routine method for measuring bond stress, steel strain, and slip in reinforced concrete beam at service loads. Magazine of concrete research. 2003, 55, No.1

Kankam, C. K. (1997). Relationship of bond stress, steel stress, and slip in reinforced concrete. Journal of Structural Engineering, vol. 123, No. 1. Jan., 1, 1997, ref. No. ST10037

Tunç, E. T., Alyamaç, K. E., İnce, R., & Ulucan, Z. Ç. (2021). Relationship between reinforcement diameter and bond stress in high performance lightweight concrete. European Journal of Science and Technology, 23, 851–860. (In Turkish, English abstract) Retrieved from https://dergipark.org.tr/en/download/article-file/1591663

Kayali, O., & Yeomans, S. R. (2000). Bond of ribbed galvanized reinforcing steel in concrete. Elsevier Science Ltd.

Yuanliang, X., Kunrong, W., Zhiyong, L., & Zhengguang, Y. (2016). Effect of coating thickness on bond behaviors of polymer cement coated plain steel bar with concrete and finite element modeling. The Open Civil Engineering Journal, 10, 571–577. https://doi.org/10.2174/1874149501610010571

Treece, R. A., & Jirsa, J. O. (1989). Bond strength of epoxy-coated reinforcing bars. ACI Materials Journal, 86(2), 104–113.

Tang, C.-W., & Cheng, C.-K. (2020). Modeling local bond stress–slip relationships of reinforcing bars embedded in concrete with different strengths. Materials, 13(17), 3701. https://doi.org/10.3390/ma13173701

Burdziński, M., & Niedostatkiewicz, M. (2022). Experimental-numerical analysis of the effect of bar diameter on bond in pull-out test. Buildings, 12(9), 1392. https://doi.org/10.3390/buildings12091392

Charles, K., Gbinu, S. K., Ogunjiofor, E. I., & Okabi, I. S. (2018). Chloride inducement on bond strength yield capacity of uncoated and resins/exudates inhibited reinforcement embedded in reinforced concrete structures. International Journal of Scientific & Engineering Research, 9(4), 874–885.

Biparva,  A. (2019). Preventing Corrosion in Reinforced Concrete - Kryton Read date 15/8/2024

Rodrigues, R., Gaboreau, S., Gance, J., Ignatiadis, I., and Betelu, S. (2021). Reinforced concrete structures: A review of corrosion mechanisms and advances in electrical methods for corrosion monitoring, Construction and Building Materials, Volume 269, 2021, 121240, ISSN 0950-0618,

https://doi.org/10.1016/j.conbuildmat.2020.121240.

NACE International. (2017). SP0188: Field Application of Fusion-Bonded Epoxy Coating to Steel Reinforcement for Concrete. NACE Int.

Prasad, D. (2021). Corrosion and Natural Corrosion Inhibitors: A Case Study for C. microphyllus. In: Corrosion [Working Title]. London: Intech Open; 2021. DOI: 10.5772/intechopen.100505

Naha, A., Islam, G. M. S., & Chowdhury, M. A. I. (2021). Bond strength of epoxy-coated reinforcement in concrete. In Proceedings of the International Conference on Planning, Architecture & Civil Engineering (pp. 112–119). Rajshahi University of Engineering & Technology.

Chen, X., & Wu, Z. (2019). Influence of polymer coating on bond and flexural strength of RC beams. Construction and Building Materials, 198, 275–283.

Buchheit, R. G. (2018). Handbook of Environmental Degradation of Materials (Third Edition), Chapter 21 – corrosion resistant coatings and paints, 2018, 449–468. doi:10.1016/B978-0-323-52472-8.00022-8.

Nguyen, T. H. and Nguyen, T. A. (2018). Protection of Steel Rebar in Salt-Contaminated Cement Mortar Using Epoxy Nanocomposite Coatings. International Journal of Electrochemistry Volume 2018, Article ID 8386426, 10 pages. https://doi.org/10.1155/2018/8386426

Sabău, M., Pop, I., & Oneț, T. (2016). Experimental study on local bond stress–slip relationship in self-compacting concrete. Materials and Structures, 49(11), 3693–3711. https://doi.org/10.1617/s11527-015-0749-5

Tang, C.-W., & Cheng, C.-K. (2020). Modeling local bond stress–slip relationships of reinforcing bars embedded in concrete with different strengths. Materials, 13(17), 3701. https://doi.org/10.3390/ma13173701

Fayette, S., Zhang, L., & Ruiz, J. (2024). Bond–slip behavior of steel reinforcing bars in ultra-high-performance concrete. Frontiers in Built Environment, 10, 1354657. https://doi.org/10.3389/fbuil.2024.1354657

Lee, H., Marino, G., & Svensson, D. (2025). Cyclic development of local bond stress in deformed rebars embedded in concrete. Journal of Structural Engineering, 151(3), 04025123. https://doi.org/10.1061/(ASCE)ST.1943-541X.0002637

Mofidi, A., Mirzabagheri, S., Doyle, A. K. K., & Chaallal, O. (2024). A novel analytical bond model for ETS FRP bars in shear rehabilitation of concrete members. International Journal of Concrete Structures and Materials, 18(81). https://doi.org/10.1186/s40069‐024‐00726‐4

Wang, J., Guo, J., & Fu, C. (2024). Steel‐concrete bond versus primary crack opening in reinforced concrete beams. KSCE Journal of Civil Engineering, 28, 5057–5065. https://doi.org/10.1007/s12205‐024‐1566‐6

Chen, Y., Yang, X., Lin, J., Xie, G., Zhang, M., & Wang, Y. (2025). Predicting bond‐slip behaviour in grouted bellows connect rebar using deep learning. Smart Construction, 2(1), 0006. https://doi.org/10.55092/sc20250006

Tang, S., Huang, W., Wang, B., & Zhou, Z. (2025). Experimental study on bond‐slip performance between H‐section steel and UHPC under monotonic and cyclic loading. Structural Engineering and Mechanics, 93(3), 195–205. https://doi.org/10.12989/sem.2025.93.3.195