| Journal Name: | Journal of Materials Science Research and Reviews |
| --- | --- |
| Manuscript Number: | Ms_JMSRR_144095 |
| Title of the Manuscript: | Recovery of silver from waste electronic printed circuit boards of cell phone and television using Organic acid |
| Type of the Article | Original Research Article |

| PART 1: Comments |  |  |
| --- | --- | --- |
|  | Reviewer’s comment Artificial Intelligence (AI) generated or assisted review comments are strictly prohibited during peer review. | Author’s Feedback (It is mandatory that authors should write his/her feedback here) |
| Please write a few sentences regarding the importance of this manuscript for the scientific community. A minimum of 3-4 sentences may be required for this part. | This manuscript is especially valuable to the scientific community because it tackles one of today’s urgent environmental and technological challenges: how to sustainably recover precious metals from electronic waste. By using environmentally friendly organic acids like oxalic and malic acid to extract silver from discarded circuit boards, the study presents a greener option to replace the harsher methods that depend on inorganic acids. The research carefully evaluates key factors such as time, temperature, and acid concentration, offering a clear look at how these conditions affect both efficiency and reaction kinetics. Most importantly, the results show that organic acids can achieve strong recovery yields while reducing environmental harm, pointing the way toward more sustainable e-waste recycling and conservation of critical metal resources. | Efficient hydrometallurgical process will contribute to diversification of metal production, reducing dependence on limited natural reserves, and promoting circular economy practices. The work will provide valuable data for optimizing the recycling of metals, enabling policymakers, waste management agencies, and recycling industries to design evidence-based strategies for e-waste handling. These research will guide the selection of eco-friendly leaching agents and process parameters that minimize environmental impact while maximizing recovery efficiency. |
| Is the title of the article suitable? (If not please suggest an alternative title) | Hydrometallurgical Recovery of Silver from Waste Printed Circuit Boards Using Oxalic and Malic Acids | Hydrometallurgical Recovery of Silver from Waste Printed Circuit Boards Using Oxalic and Malic Acids. I see this tittle better than Recovery of silver from waste electronic printed circuit boards of cell phone and television using Organic acid |
| Is the abstract of the article comprehensive? Do you suggest the addition (or deletion) of some points in this section? Please write your suggestions here. | The study was aimed at recovering silver from waste printed circuit boards of cell phones and televisions using two different organic acids. The metallic parts of the waste printed circuit boards of cell phones and televisions were separated, washed with sodium hydroxide, dried, pulverized to 75 µm, and then characterized using SEM- EDX and XRD. The leaching experiment was carried out with different concentrations of oxalic and malic acids, at different time intervals and temperatures. Leaching efficiency was determined by analyzing the leached solution with an atomic absorption spectrophotometer. The SEM result shows a magnified view of the material's surface and the presence of metal particles in the PCB samples of cell phones, while a rough, irregular surface with a combination of smooth and textured areas was observed for waste PCBs of televisions. The EDX result recorded a weight concentration of 1.06 wt% and 3.51 wt% for cell phone and television respectively. Moreover, oxalic acid recorded the highest yield (83.47%) at 30 °C, which was the optimum temperature. The optimum leaching time was 2 hr with 73.85% efficiency, while the optimum concentration was 4 M. The kinetic study shows that both acids fit the pseudo-first order model reasonably well, with malic acid giving a better correlation. For television PCBs, oxalic acid showed an excellent fit (R² ≈ 0.90). Considering the rate constants (K1), the study reveals that malic acid dissolves Ag faster from waste PCBs of cell phones. The work also shows that the extraction of Ag from televisions with oxalic acid is spontaneous at all tested temperatures. (There are some errors in the use of grammar I corrected that) | Electronic waste (e-waste) is growing rapidly worldwide and represents a significant environmental threat due to technological advancements. The environmental impacts of e-waste disposal are gaining increasing global attention. Recovery methods used in developing countries often expose people to numerous toxic materials and contaminants. This study aimed to recover silver from waste printed circuit boards (PCBs) of cell phones and televisions using two organic acids. The metallic parts of the waste PCBs from cell phones and televisions were separated, washed with sodium hydroxide, dried, pulverized to 75 µm, and characterized using SEM-EDX and XRD. Leaching experiments were conducted with varying concentrations of oxalic and malic acids, different time intervals, and temperatures. Leaching efficiency was determined by analyzing the leached solution using an atomic absorption spectrophotometer. SEM analysis revealed a magnified view of material's surface and also presence of metal particles in the PCB samples of cell phone and a rough, irregular surface with a combination of smooth and textured areas for waste PCB of television. EDX analysis indicated silver weight concentrations of 1.06% and 3.51% for cell phone and television PCBs, respectively. Silver from cell phone PCBs leached with 3 M oxalic acid achieved the highest yield (83.47%) at 30°C and 3 hours, representing the optimal condition. Malic acid under the same conditions yielded 63.77%. For television PCBs, silver leaching with oxalic acid recorded the highest efficiency of 73.88% at 30°C and 3 hours, while malic acid achieved 35.74% under the same conditions. Kinetic studies showed that both acids fit pseudo-first- and pseudo-second-order models reasonably well, with malic acid providing a better correlation. For television PCBs, oxalic acid exhibited an excellent fit (R² ≈ 0.90). Rate constants (k₁) indicated that malic acid dissolved silver faster from cell phone PCBs. The green leaching of silver from end-of-life PCB panels using organic acids offers an environmentally beneficial approach. |
| Is the manuscript scientifically, correct? Please write here. | Yes, the manuscript is scientifically correct | Yes, the manuscript is scientifically correct |
| Are the references sufficient and recent? If you have suggestions of additional references, please mention them in the review form. | More recent references should be added | The references have been edited |
| Is the language/English quality of the article suitable for scholarly communications? | Yes | Yes |
| Optional/General comments | Work on the grammar part | That has been edited |

| PART 2: |  |  |
| --- | --- | --- |
|  | ## Reviewer’s comment | Author’s Feedback (It is mandatory that authors should write his/her feedback here) |
| Are there ethical issues in this manuscript? | (If yes, Kindly please write down the ethical issues here in details) |  |