Effect of whitening dentifrice containing blue covarine on the color of enamel stained with different beverages

ABSTRACT

Aims: evaluate the effect of whitening dentifrice containing BC on the color of enamel stained with different beverages. Study design: Mention the design of the study here. Place and Duration of Study: Experimental in vitro study, comparative, with parallel groups, controlled, and randomized Methodology: Fifteen molars were sectioned to obtain enamel specimens, which were flattened, and divided into 6 groups: distilled water, cola-based soft drink, wine, acai, coffee, and dark beer. The color of the specimens was evaluated using a spectrophotometer. Subsequently, they were immersed in the beverages for 6 hours/day, for a total of 30 days. Each specimen was inserted into a brushing machine containing a solution with BC. All data were analyzed by ANOVA and the Student-Newman-Keuls test (α=0.05). Results: As for Δb*, no statistical difference was observed among the distilled water, cola-based soft drink, wine, and coffee groups (p>0.05). Also, no statistical difference was found between the acai and dark beer groups (p>0.05).splenic diameter ratio (1676.7 to 824.6) declining significantly. Logistic regression showed splenic collaterals and platelets are significantly but negatively associated with esophageal varices grades. Conclusion: The whitening dentifrice containing BC was effective in altering the color of tooth enamel stained with coffee, the cola-based soft drink, wine, acai, and dark beer.

Keywords: Blue covarine, Dentifrices, Tooth bleaching, Biomaterials.

1. INTRODUCTION

The occurrence of extrinsic enamel staining and tooth darkening are problems constantly reported by patients who seek esthetic improvements in their smile. The frequent consumption of beverages containing high concentrations of organic pigments, such as tea, coffee, acai, wine, and cola-based soft drinks, can lead to tooth staining (Çelik et al., 2021, Zanatta et al., 2016, Soares et al., 2015).

Due to the increased demand of patients seeking white and stain-free teeth, the dental products industry has launched mouthwashes and dentifrices that claim to whiten teeth (Kwon et al., 2015, Andrade et al., 2021, Meireles et al., 2021, Borges et al., 2023).

However, there are controversies regarding the safety of these types of dentifrices, mainly regarding the risk of irreversible damage to the tooth enamel due to the abrasive action of their components (Carey, 2014).

Although teeth whitening is a procedure desired by patients who are dissatisfied with the color of their teeth, it usually has a high cost, leading many patients to seek more affordable alternatives (Santos et al., 2024). As an alternative to whitening dentifrices with abrasive action, toothpastes containing blue covarine (BC) have been developed. The primary mechanism of action of these products is based on optical effects promoted by the deposition of a thin layer of BC on the surface of the tooth enamel. This pigment has the ability to attenuate the perception of yellow color and bring out bluish tones, resulting in an optical illusion of greater luminosity of the teeth. The decrease in yellow color is an important indicator in tooth whitening and is a relevant parameter to the patient regarding self-perception (Hashemikamangar et al., 2020, Vaz et al., 2019).

Although it has been proven that after brushing with a dentifrice containing BC, there is a whitening effect, there are still gaps in scientific knowledge concerning its efficiency. According to coloring and acidic beverages, such as cola-based soft drinks, coffee, red wine, dark beer, and acai, promote significant changes in the color of tooth enamel. Thus, it remains to be elucidated whether dentifrices containing BC are efficient in attenuating or masking different types of extrinsic enamel staining (Bortolatto et al., 2016, Neri et al., 2020).

In this context, the aim of the present study was to evaluate the effect of a whitening dentifrice containing BC on the color of enamel stained with different beverages: wine, acai, dark beer, and a cola-based soft drink. The null hypotheses tested were that there would be no statistical difference among the groups regarding the values of ΔL*, Δa*, Δb*, and ΔE*.

2. material and methods

This study was approved by the Human Research Ethics Committee (No. 2,758,761). Fifteen healthy human third molars were selected, cleaned, and stored in distilled water at 4°C. The teeth were fixed with wax (Kota Ind. e Com. Ltda., São Paulo, SP, Brazil) on acrylic plates and placed into a cutting machine (Extec, Enfield, CT, USA), where they were cut with the aid of a diamond disk (Extec Corp, Enfield, CT, USA) to obtain 4 mm x 4 mm enamel fragments.

The enamel fragments were embedded (PRE30Mi; Arotec, São Paulo, SP, Brazil) in acrylic resin and later flattened and polished with 320, 400, 600, and 1200 silicon carbide sandpaper grits. Each step of the flattening and polishing process was carried out for 60 seconds.

All specimens were analyzed with a 40X magnification stereoscopic magnifying glass (StereoZoom® Leica S8 APO, Leica Microsystems, Wetzlar, Germany) to ensure that they were exclusively enamel, without cracks, and without exposed dentin areas. Subsequently, the specimens were randomly divided using the Excel program (Excel 2019, Microsoft Corporation, One Microsoft Way, Redmond, WA, USA) into 6 groups (n=5), according to the evaluated beverages: distilled water (control), cola-based soft drink, wine, acai, coffee, and dark beer.

Initially, the color of each specimen was assessed (baseline) with the aid of a spectrophotometer (VITA Easyshade® Advance 4.0, Vident, Brea, CA, USA) and, afterward, they were individually submerged in 5 mL of the respective beverage at 37°C for 6 hours/day, for up to a total of 30 days. In the immersion intervals, the samples were maintained in artificial saliva at 37°C. The coffee was prepared, according to the manufacturer’s instructions, in the proportion of 8 mg of ground coffee in 50 mL of warm water. As for the acai preparation, 100 g of pulp was used in 200 mL of ice water, according to the manufacturer’s instructions. In order to prevent possible chemical alterations in the beverages, they were replaced every 24 hours (Karadas M, Seven N, 2014).

After 30 days, the specimens were removed from the vials containing the coloring beverage and washed with distilled water for 20 seconds. Subsequently, they were carefully dried with a water- and oil-free air blaster for 10 seconds, after which an intermediate evaluation was conducted using a spectrophotometer.

Each specimen was inserted in a mechanical brushing machine (Brushing machine - XY movement, Biopdi, São Carlos, SP, Brasil) and immersed in 5 mL of a solution containing BC-based whitening dentifrice (Close Up White Now Glacier Fresh; Unilever, São Paulo, SP, Brazil), artificial saliva, and distilled water, obtained by diluting equal volumes of each component (1:1:1). Next, the specimens were subjected to brushing with a soft-bristled toothbrush for 3,150 cycles (150 strokes/minute, 3 minutes/day, for 7 days, with a 200 g load), using a horizontal brushing technique, simulating the toothbrushing recommendations given to patients: 3 times per day, for 1 min. After each cycle, the specimens were washed in running water and stored in artificial saliva.

After brushing, a final evaluation was carried out with a spectrophotometer that measured color using values corresponding to the CIE L* a* b* scale. In this system, L* indicates luminosity, and a* and b* the hue, with a* representing saturation on the red-green axis and b* on the blue-yellow axis.

The comparison of color before and after the specimens were exposed to the beverages and the brushing procedure was based on the color difference or ΔE, represented by the equation:

ΔE ab = [(ΔL )2 + (Δa )2+ (Δb )2 ]0.5

All of the specimens’ color spectra readings were standardized regarding the location of the evaluated specimen, luminosity, temperature, and ambient humidity. The measuring aperture was set and positioned perpendicularly to the enamel surface. When the value of ΔE was greater than 3.7, the color variation was considered easily clinically visible. Values between 3.7 and 1 were considered a clinically acceptable color difference. On the other hand, ΔE values less than 1 were considered clinically imperceptible ( Reis et al., 1996).

Statistical analysis was performed using the SigmaStat 3.5 program (Systat Software Inc., San Jose, CA, USA). All data were analyzed using the Analysis of Variance (ANOVA) test, and post-hoc comparisons were conducted using the Student-Newman-Keuls test. The adopted level of significance was p<0.05.

3. results and discussion

Enamel color evaluation after immersion in coloring beverages

The data obtained from the evaluation of the parameters ΔL, Δa, Δb, and ΔE are shown in Table 1.

Analysis of ΔL values (variation in brightness)

All groups presented negative results, indicating that the specimens became darker after exposure to the beverages. No statistical difference was observed among the samples exposed to distilled water, the cola-based soft drink, and dark beer (p>0.05). Those exposed to wine, acai, and coffee had significantly lower ΔL values (p<0.05); therefore, they became darker than specimens from the other groups.

Analysis of Δa values (red-green axis variation)

There was no statistical difference among the Δa values of all groups tested (p>0.05). All groups had positive Δa results, indicating a shift in the color of the specimens to the red spectrum.

Analysis of Δb values (yellow-blue axis variation)

The specimens exposed to wine presented negative Δb values, denoting a color shift to the blue spectrum. The wine group had significantly lower Δb values compared to the cola-based soft drink, coffee, and dark beer groups (p<0.05). Nonetheless, there was no statistical difference among the distilled water, cola-based soft drink, acai, coffee, and dark beer groups (p>0.05).

Analysis of ΔE values (total color variation)

The lowest ΔE values were observed in the distilled water group (p<0.05). No statistical difference was found among the ΔE values of the specimens stained with the cola-based soft drink, wine, acai, and coffee (p>0.05). However, there was a significant difference between the wine and dark beer groups (p<0.05). All groups, with the exception of the distilled water group, had a ΔE greater than 3.7; therefore, they presented clinically visible color variations.

Enamel color evaluation after treatment with BC

The data obtained from the evaluation of the parameters ΔL*, Δa*, Δb*, and ΔE* are shown in Table 2.

Analysis of ΔL* values (variation in brightness)

There was no statistical difference among groups (p>0.05).

Analysis of Δa* values (red-green axis variation)

No statistical difference was observed among the tested groups regarding the Δa* values (p>0.05). All groups had positive Δa* results, indicating a shift in the color of the specimens to the red spectrum.

Analysis of Δb* values (yellow-blue axis variation)

There was no statistical difference among the distilled water, cola-based soft drink, wine, and coffee groups (p>0.05), nor was there a statistical difference between the acai and dark beer groups (p>0.05). However, a significant difference was observed between the distilled water and dark beer groups (p<0.05). The latter group presented negative Δb* results, denoting a color variation in the blue spectrum; the other groups had positive values, indicating variations in the yellow spectrum.

Analysis of ΔE* values (total color variation)

No statistical difference was observed among the groups (p>0.05). The ΔE* values of all groups were greater than 3.7; therefore, there was a clinically visible change in color after exposure to BC.

3.1 Discussion

Some studies show that a diet based on the frequent consumption of foods with high levels of pigmenting agents directly influences the color of tooth enamel, which can lead to extrinsic stains. When evaluating the Δb values of the groups of samples stained with the cola-based soft drink, wine, and coffee, it was noted that they were statistically equal to the control group (distilled water), a fact that would explain the reduction in the yellow color of the teeth after brushing. Our findings contrast with those reported in the study by Torres et al., who tested the effectiveness of mouthwashes and dentifrices in changing the enamel tonality after coffee staining ( Taneja et al., 2016, Proctor et al., 2005, Torres et al., 2013).

The authors found that the subjective level of responses to improvement and satisfaction with the whiteness were significantly associated with changes in Δb values, but not with alterations in ΔL and Δa values, corroborating the present study, which demonstrated statistical changes only in the yellow-blue spectrum.

Considering the importance of reducing the Δb value in tooth whitening, it is understood that the deposition of blue-colored agents on the enamel surface would give rise to favorable changes in the optical properties of the tooth, particularly in the color change to blue, improving the measurement and perception of tooth whitening.

Tooth whitening products are marketed in many different formats (Gerlach et al., 2001). However, dentifrices comprise the most affordable product format for many patients and consumers. Therefore, the incorporation of BC in dentifrice formulations has been investigated in several studies. Collins et al. and Joiner et al. showed immediate and noticeable results that lasted for up to 8 hours after a single application of their tested product, whereas Torres et al., 2013,  Dantas et al., 2015, Oliveira et al., 2016, Horn et al., 2014 and Bortolatto et al 2016 were unable to evidence superior whitening effects to those provided by a conventional toothpaste, a fact that contrasts with the results found herein, seeing that a statistical change in the Δb value was observed.

Finally, when evaluating the color stability of the tooth enamel after immersion in dark beer and brushing with BC, it was noted that its Δb was significantly influenced by the oral hygiene process, a fact that can be explained by the change in the enamel color to the blue spectrum in an attempt to balance the yellowish color after immersion in the coloring beverage. These findings demonstrate the efficiency of BC at changing the color of the tooth enamel since the coloration of teeth stained with dark beer had statistically equal results to non-stained teeth after brushing.

4. Conclusion

The whitening dentifrice containing BC was efficient in changing the color of tooth enamel stained with coffee, the cola-based soft drink, wine, acai, and dark beer, acting primarily in the balance of the blue and yellow spectra.

ETHICAL APPROVAL

The research was approved by the research ethics committee of the fortaleza university, according to opinion number 2,758,761.

References

Çelik ZC, Çakiris A, Yanıkoğlu F, Abacı N, Ekmekçi SS, Ilgın C, et al. Metagenomic analysis of black-stained plaques in permanent dentition. Archives of Oral Biology 2021;128:105171

Zanatta RF, Esper MÂLR, Valera MC, Melo RM, Bresciani E. Harmful Effect of Beer on Bovine Enamel Microhardness – In Vitro Study. PLoS ONE 2016;11:e0163440

Soares CNGS, Amaral BLF, Mesquita FM, Franca GMF, Basting TR, Turssi PC. Toothpastes containing abrasive and chemical whitening agents: Efficacy in reducing extrinsic dental staining. General Dentistry 2015;63(6), 24–28

Kwon SR, Wertz PW. Review of the Mechanism of Tooth Whitening: The Mechanism of Tooth Whitening. J Esthet Restor Dent 2015;27:240–57.

Andrade ICGB, Silva BM, Turssi CP, Amaral FLB, Basting TR, Souza EM, et al.  Effect of whitening dentifrices on color, surface roughness and microhardness of dental enamel in vitro. Am J Dent 2021; 34(6):300-306.

Meireles SS, Sousa JP, Lins RBE, Smapaio FC. Efficacy of whitening toothpaste containing blue covarine: A double-blind controlled randomized clinical trial. J Esthet Restor Dent 2021;33(2):341-350.

Borges  JS, Soares CJ, Bragança GF, Vilela ABF, Soares PBF. Effect of Activated Charcoal Toothpaste on Color Stability of Bleached Teeth Immersed in Different Drinks. Oper Dent 2023;1;48(2):207-217.

Carey CM. Tooth Whitening: What We Now Know. Journal of Evidence Based Dental Practice 2014;14:70–6.

Santos ME, Silva ROD, Cavalcanti YW, Meireles SS. At-home bleaching versus whitening toothpastes for treatment of tooth discoloration: a cost-effectiveness analysis. J Appl Oral Sci. 2024 Feb 5;32:e20230336.

Hashemikamangar SS, Hoseinpour F, Kiomarsi N, Dehaki MG, Kharazifard MJ. Effect of an Optical Whitening Toothpaste on Color Stability of Tooth-Colored Restorative Materials. Eur J Dent 2020;14:085–91.

Vaz VTP, Jubilato DP, Oliveira MRM, Bortolatto JF, Floros MC, Dantas AAR, et al. Whitening toothpaste containing activated charcoal, blue covarine, hydrogen peroxide or microbeads: which one is the most effective? J Appl Oral Sci 2019;27:e20180051.

Bortolatto JF, Dantas AAR, Roncolato Á, Merchan H, Floros MC, Kuga MC, et al. Does a toothpaste containing blue covarine have any effect on bleached teeth? An in vitro, randomized and blinded study. Braz Oral Res 2016;30.

Neri JR, Aragão LR, Nigri FMN, Passos VF, Barros LO, Sampaio FA, et al. Efeito de bebidas corantes e ácidas na estabilidade da cor do esmalte dentário após clareamento de consultório. Acervo Saúde 2020;12:e2594.

Karadas M, Seven N. The effect of different drinks on tooth color after home bleaching. Eur J Dent 2014;08:249–53.

Reis RS, Neiva GF, Yaman P, Razzoog ME. Effect of Firing on the Color Stability of a Light-Cured Ceramic Stain. J Prosthodontics 1996;5:182–5.

Taneja S, Kumar M, Agarwal P, Bhalla A. Effect of potential remineralizing agent and antioxidants on color stability of bleached tooth exposed to different staining solutions. J Conserv Dent 2018;21:378.

Proctor GB, Pramanik R, Carpenter GH, Rees GD. Salivary Proteins Interact with Dietary Constituents to Modulate Tooth Staining. J Dent Res 2005;84:73–8.

Torres C, Perote L, Gutierrez N, Pucci C, Borges A. Efficacy of Mouth Rinses and Toothpaste on Tooth Whitening. Operative Dentistry 2013;38:57–62.

Gerlach RW, Zhou X. Vital Bleaching with Whitening Strips: Summary of Clinical Research on Effectiveness and Tolerability. The Journal of Contemporary Dental Practice 2001;2:28–42.

Collins LZ, Naeeni M, Platten SM. Instant tooth whitening from a silica toothpaste containing blue covarine. Journal of Dentistry 2008;36:21–5

Joiner A, Philpotts CJ, Alonso C, Ashcroft AT, Sygrove NJ. A novel optical approach to achieving tooth whitening. Journal of Dentistry 2008;36:8–14.

Dantas AAR, Bortolatto JF, Roncolato Á, Merchan H, Floros MC, Kuga MC, et al. Can a bleaching toothpaste containing Blue Covarine demonstrate the same bleaching as conventional techniques? An in vitro, randomized and blinded study. J Appl Oral Sci 2015;23:609–13.

Oliveira M, Fernández E, Bortolatto J, Oliveira Junior O, Bandeca M, Khajotia S, et al. Optical Dental Whitening Efficacy of Blue Covarine Toothpaste in Teeth Stained by Different Colors: Optical Dental Whitening Efficacy. J Esthet Restor Dent 2016;28:S68–77.

Horn BA, Bittencourt BF, Gomes OMM, Farhat PA. Clinical Evaluation of the Whitening Effect of Over-the-Counter Dentifrices on Vital Teeth. Braz Dent J 2014;25:203–6.

Table 1.

Mean values of color coordinates (ΔL, Δa, Δb and ΔE) of enamel after immersion in coloring beverages.

| Groups (n=5) | ΔL | Δa | Δb | ΔE |
| --- | --- | --- | --- | --- |
| Distilled water | -1.62±4.65A | 2.38±2.06A | 2.46±2.59AB | 3.79±2.70A |
| Cola-based soft drink | -4.16±6.53A | 4.12±5.24A | 13.10±3.83A | 16.28±3.26BC |
| Wine | -19.84±5.35B | 4.02±2.98A | -6.06±9.59B | 23.32±2.53B |
| Acai | -18.54±5.49B | 5.20±2.89A | 2.36±7.21AB | 20.98±3.81BC |
| Coffee | -12.68±5.11B | 6.86±1.02A | 8.00±10.17A | 18.86±5.08BC |
| Dark beer | -5.22±3.24A | 4.46±1.82A | 9.18±10.23A | 13.94±6.31C |

*Identical superscript letters indicate no statistical significance between values in columns.

Table 2.

Mean values of color coordinates (ΔL *, Δa *, Δb * and ΔE *) of enamel after treatment with dentifrice containing blue covarine.

| Grupos (n=5) | ΔL* | Δa* | Δb* | ΔE* |
| --- | --- | --- | --- | --- |
| Distilled water | 6.40±5.82A | 2.92±3.20A | 14.96±2.85A | 17.49±3.33A |
| Cola-based soft drink | 3.08±6.19A | 4.66±2.10A | 10.28±2.79AB | 13.13±2.44A |
| Wine | -3.32±11.69A | 4.66±5.03A | 11.98±8.75AB | 18.94±3.25A |
| Acai | -6.12±4.72A | 4.50±3.25A | 0.26±8.26BC | 11.28±3.76A |
| Coffee | 3.48±6.41A | 5.88±3.18A | 11.88±5.88AB | 15.07±6.05A |
| Dark beer | -6.40±9.38A | 1.70±2.46A | -6.02±10.69C | 14.88±5.61A |

*Identical superscript letters indicate no statistical significance between values in columns.