Phytochemical-Assisted Synthesis of Silver Nanoparticles using Eucalyptus Leaf Extract: Structural Characterization and Antimicrobial Evaluation

## Abstract

The search for safer and environmentally friendly nanoparticle-synthesis methods is becoming more prominent in sustainable nanotechnology. In this study, phytochemical-assisted green synthesis of silver nanoparticles (AgNPs) was achieved using Eucalyptus globulus leaf extract (ELE), a rich source of phenolics, flavonoids, and tannins. The ELE concentrations ranging from 1–6% w/v provided differential phytochemical availability, directly influencing nanoparticle nucleation, growth, and stabilization. UV–Vis spectroscopy confirmed surface plasmon resonance bands at 420-422 nm responsible for AgNPs. FTIR analysis confirmed the presence of O–H, C=O, and C=C functional groups responsible for both reduction and capping of the AgNPs. TEM imaging demonstrated a concentration-dependent decrease in particle agglomeration, with 6% w/v ELE producing predominantly spherical nanoparticles averaging 12.90 nm. XRD analysis indicated crystalline face-centred cubic structures of AgNPs. Antibacterial assays showed significant inhibitory activity against Staphylococcus aureus and Klebsiella pneumoniae, with MIC values surpassing those of Neomycin. These findings established that phytochemical-assisted green synthesis of AgNPs has a promising antimicrobial potential against the pneumonia-causing pathogens with controlled morphology and bioactivity.

Keywords: Green Synthesis, Eucalyptus globulus, Silver Nanoparticles, Phytochemicals, Antimicrobial Activity

# 1.0 Introduction

Nanotechnology has emerged as one of the most transformational scientific fields of the twenty-first century, enabling modification of material into nanoscale and design of unique, functional structures [1,2]. Among the several nanomaterials investigated, silver nanoparticles (AgNPs) have sparked great interest due to their distinct physicochemical and biological properties. AgNPs possess excellent antibacterial activities, catalytic efficiency, and unique optical features due to their surface plasmon resonance [3]. These features render them promising for diverse biomedical, environmental, agricultural, and industrial applications [4]. Biomedical applications include wound healing, antimicrobial coatings, biosensors, medication delivery systems, food packaging, and water treatment [3–7]. The broad applicability of AgNPs arises from their high surface area-to-volume ratio, enhancing reactivity and enabling molecular and cellular interactions unattainable with bulk materials [8].

Despite their advantages, conventional techniques for synthesizing AgNPs present significant limitations. Methods such as chemical reduction, laser ablation, and evaporation–condensation typically involve toxic reducing agents, high energy inputs, and generate hazardous byproducts that threaten both environmental and human health, thereby posing major challenges for sustainable large-scale production [9,10]. These concerns have driven the exploration of alternative synthesis pathways aligned with the principles of green chemistry, emphasizing renewable resources, reduced toxicity, and lower energy requirements [11]. In response, green nanotechnology seeks to develop eco-friendly, economically feasible, and biocompatible methods for nanoparticle production, including phytochemical-mediated synthesis using plant extracts, microbial-assisted approaches employing bacteria and fungi, and biopolymer-based strategies utilizing natural polysaccharides such as chitosan and starch [12].

Plant-mediated nanoparticle synthesis has however, gained prominence due to the abundance of secondary metabolites such as polyphenols, flavonoids, tannins, alkaloids, and terpenoids that act as natural reducing and stabilizing agents [13]. These biomolecules facilitates the conversion of silver ions (Ag⁺) into metallic silver (Ag⁰) while preventing nanoparticle agglomeration [14]. Microbial assisted-synthesis on ther other hand demand stringent sterile conditions and long-term culture preservation [15]. Besides cost-effectiveness, plant-derived phytochemicals impart additional biological functionality to the nanoparticles, enhancing their antibacterial, antioxidant, and catalytic properties [16,17].

Over the past two decades, numerous plants have been investigated for the green synthesis of AgNPs, primarily due to their diverse phytochemical constituents [15]. Azadirachta indica was among the earliest reported, where metabolites such as azadirachtin, flavonoids, and terpenoids facilitated the formation of AgNPs sized 50–100 nm [18,19]. Aloe vera, enriched with anthraquinones, phenolics, and polysaccharides, produced spherical AgNPs ranging from 10–40 nm [20]. Similarly, Ocimum sanctum, containing eugenol and ursolic acid, yielded AgNPs of 20–50 nm [21]. Moringa oleifera seeds and leaves also produced AgNPs of 15–25 nm [22].

Among explored species, Eucalyptus has emerged as particularly important due to its global distribution and reservoir of bioactive phytochemicals such as 1,8-cineole, tannins, flavonoids, phenolic acids, and terpenoids [23,24]. These compounds not only provide medicinal benefits but also act as efficient reducing and stabilizing agents. Several studies have highlighted its effectiveness in producing stable, monodispersed AgNPs. For instance, Sadiq et al.[25] reported spherical AgNPs of 30–50 nm synthesized from Eucalyptus globulus, while Ali et al.[26] achieved smaller nanoparticles of 1.9–4.3 nm under microwave-assisted synthesis. However, the relationship between extract concentration, phytochemical availability, and nanoparticle nucleation and morphology remains poorly established in Eucalyptus-based synthesis. Moreover, comprehensive structural characterization and systematic evaluation of concentration-dependent antibacterial activity against clinically relevant pathogens are rarely addressed.

The aim of this study was to synthesize silver nanoparticles using ELE, investigate the effect of extract concentration on particle size and morphology, evaluate their optical and structural properties, and assess their antimicrobial potential against S. aureus and K. pneumoniae, pneumonia-causing microorganisms.

# 2.0 Materials and Methods

## 2.1 Materials

Fresh leaves of Eucalyptus globulus were collected in November 2024 from the botanical garden of Maasai Mara University, Narok County, Kenya (1°06′20″ S, 35°52′10″ E). Other chemicals were Silver nitrate (AgNO₃, ≥99.8%), Methanol (CH₃OH, ≥99.5%), Sodium tripolyphosphate (Na₅P₃O₁₀, ≥95%), Tween 80 (C₆₄H₁₂₄O₂₆), Sodium hydroxide (NaOH, ≥98%), Folin–Ciocalteu reagent, Gallic acid (C₇H₆O₅, ≥97.5%, Aluminum chloride (AlCl₃, ≥98%), Quercetin (C₁₅H₁₀O₇, >95.5%), Sodium carbonate (Na₂CO₃, ≥99%, Ferric chloride (FeCl₃, ≥97%), Hydrochloric acid (HCl, 32%), Dragendorff's reagent, Copper acetate monohydrate (Cu(CH₃COO)₂·H₂O, ≥98%), Anhydrous Magnesium sulphate (MgSO₄, ≥99%), Ethanol (C₂H₅OH,  ≥99.8%), Sodium nitrite (NaNO₃, ≥99.0%). All the chemicals were purchased from Sigma Aldrich and were of analytical grade. Nutrient broth, Muller Hinton Agar, and the bacteria culture were obtained from the Biology laboratory, Maasai Mara University. Distilled water was used throughout the experiments.

## 2.2 Methods

### 2.2.1 Sample pretreatment

The fresh Eucalyptus globulus leaves were collected from healthy, mature trees and thoroughly inspected to remove diseased, insect-infested or physically damaged leaves. The leaves were first rinsed with running tap water to eliminate dust and surface impurities, followed by washing with distilled water to remove residual contaminants. The cleaned leaves were air-dried at room temperature (25 ± 2 °C) for 48 hours in a shaded and dust-free environment within the laboratory. After drying, the leaves were oven-dried at 40–45 °C until constant weight was achieved to minimize moisture content and prevent microbial growth. The dried leaves were then crushed into powder using a sterile mechanical grinder, transferred into sterile, airtight polythene bags, and stored at room temperature in a dry, dark cabinet for further experiments.

2.2.2 Preparation of the Eucalyptus leaf extract

To prepare 1% w/v ELE, the pre-treated Eucalyptus leaf powder (1.0 g) was accurately weighed using an analytical balance and transferred into a 100 mL Erlenmeyer flask. Subsequently, 100 mL of distilled water was added to the flask and fited with a stopper. The mixture was then heated at 90 °C for 5 minutes to promote the extraction of bioactive phytochemicals. After heating, the extract was allowed to cool to approximately 70 °C and filtered through Whatman No.1 filter paper. The filtrate was then collected and preserved at 4 °C under refrigeration, which was maintained for three days before use. The same procedure was repeated for the 3%, and 6% w/v ELE.

### 2.2.2 Phytochemical Screening of Eucalyptus Leaf Extract

Phytochemical screening of the ELE was carried out following standard qualitative and quantitative procedures described by Shaikh & Patil [27] with slight modifications. Before analysis, the leaf extract was dissolved in 95% ethanol for assays requiring organic solvents, while emulsification with 0.5% (v/v) Tween-20 was employed for tests necessitating aqueous conditions. All analyses were performed in triplicate to ensure reproducibility, and appropriate reagent blanks and standards were included.

### 2.2.3 Determination of Total Phenolic Content (TPC)

The total phenolic content of the leaf extract was quantified using the Folin–Ciocalteu colorimetric method [28,29]. Briefly, aliquots of the extract at different concentrations (25–100 µg/mL) were prepared in methanol. To 0.5 mL of each sample, 2.5 mL of 10% (v/v) Folin–Ciocalteu reagent was added, followed by 2.0 mL of 7.5% (w/v) sodium carbonate solution after a 5-minute reaction period. The mixtures were incubated at room temperature for 30 minutes in the dark, after which absorbance was measured at 765 nm against a reagent blank. A calibration curve was prepared using gallic acid as a standard, and the total phenolic content was expressed as milligrams of gallic acid equivalents per gram of dry extract (mg GAE/g). The values were calculated using Equation 3.1.

(3.1)

where Tp ​ is the total phenolic content, C is the concentration determined from the calibration curve (mg/mL), V is the volume of extract (mL), and M is the mass of dry extract (g).

### 2.2.4 Determination of Total Flavonoid Content (TFC)

The total flavonoid content was determined using the aluminum chloride colorimetric method [30]. A standard calibration curve was prepared using quercetin solutions (25–100 µg/mL) in methanol. For the assay, 1 mL of the ELE was mixed with 4 mL of distilled water, followed by 0.3 mL of 5% (w/v) sodium nitrite solution. After 5 minutes, 0.3 mL of 10% (w/v) aluminum chloride was added, then 2 mL of 1 M sodium hydroxide was introduced after 6 minutes, and the final volume was adjusted to 10 mL with distilled water. The solution was thoroughly mixed, and absorbance was read at 415 nm against a reagent blank. Results were calculated using the quercetin calibration curve and expressed as milligrams of quercetin equivalents per gram of dry extract (mg QE/g) according to Equation 3.2 below.

(3.2)

where Tf​ is the total flavonoid content, C is the concentration obtained from the calibration curve (mg/mL), V is the volume of extract (mL), and M is the mass of dry extract (g).

### 2.2.5 Phytochemical-assisted green synthesis of silver nanoparticles

1 M AgNO₃ stock solution was prepared by dissolving 1.7 g of AgNO₃ in 10 mL of deionized water. From this stock, 2 mM AgNO₃ working solution was obtained by diluting 2 mL of the 1 M solution to a final volume of 1 L with distilled deionized water. The phytochemical-assisted synthesis of AgNPs was carried out using a reaction mixture with AgNO₃ to ELE ratio of 4:1, adjusted to pH 10 usig 0.1M NaOH. The ELE was added in aliquots of 0.5 mL under continuous stirring while maintaining the reaction temperature between 50–70 °C. During the process, the reaction mixture exhibited a distinct color transition from colorless to yellow, and finally to dark brown, indicating the formation of AgNPs. The reaction mixture was allowed to stand undisturbed for 38 hours to facilitate nanoparticle stabilization. The supernatant was then carefully decanted, leaving behind the solid deposits, which was subsequently dispersed in methanol and incubated for 12 hours to remove residual impurities. Subsequently, the methanol phase was carefully decanted, and the AgNPs were preserved in a minimal volume of methanol for characterization, followed by drying prior to further analyses.

Figure 1: Schematic presentation of the phytochemical-assisted green synthesis of AgNPs using ELE.

## 2.3 Characterization

The optical properties of AgNPs synthesized using different ELE concentrations of 1%, 3%, and 6% w/v were characterized using a Shimadzu UV-3150 spectrophotometer at room temperature. Absorption spectra were collected in the 200–800 nm range with a 1 cm path-length cuvette, using distilled water as reference. Surface plasmon resonance (SPR) peak was used to confirm the nanoparticle formation and stability across the three concentrations.

Fourier Transform Infrared (FTIR) spectroscopy was performed on the leaf extract and the across the three concentrations using a Perkin Elmer spectrometer with an attenuated total reflectance (ATR) accessory. Spectra were recorded between 4000–500 cm⁻¹ at a resolution of 4 cm⁻¹ with 32 scans averaged per sample. The spectra were baseline-corrected and normalized to identify characteristic peaks of functional groups associated with nanoparticle stabilization.

Transmission Electron Microscopy (TEM, JEOL JEM-2100) operating at 200 kV was used to assess nanoparticle size, shape, and morphology. The samples were dispersed in ethanol and sonicated for 15 minutes, deposited onto carbon-coated copper grids, and air-dried before imaging. Surface morphology was further examined using a JEOL IT-7500LA Scanning Electron Microscope at 15–20 kV. Samples were gold-sputtered to enhance conductivity, and micrographs were captured between 1,000x and 50,000x magnification to evaluate particle uniformity, surface texture, and aggregation. X-ray Diffraction (XRD) was performed using a Shimadzu XRD-7000 with Cu Kα radiation (λ = 1.5406 Å) at 40 kV and 30 mA. Scans were run from 10° to 80° (2θ) at 2°/min, and the resulting diffraction patterns were compared with the reference JCPDS card, and the average crystallite size was calculated using the Scherrer equation (Eq.3.3).

(3.3)

In the equation above K is the correction factor, which is typically set to 0.91, D is the average crystallite size,  is the line broadening in radians, θ is the Bragg angle, and λ is the X-ray wavelength.

## 2.4 Antimicrobial Tests

### 2.4.1 Determination of antimicrobial activity of the prepared samples

The antibacterial activity of the AgNPs prepared at different ELE concentrations of 1%, 3%, and 6% w/v was evaluated against S. aureus and K. pneumoniae using the minimum inhibitory concentration (MIC) method. Neomycin was used as a positive control for comparison.

### 2.4.2 Bacteria, medium, and cultivation

Bacterial strains of interest were cultivated in Brain Heart Infusion (BHI) broth, a nutrient-rich medium that simulates physiological conditions. Cultures were centrifuged at 11,000 rpm for 5 min, after which the supernatant was discarded. The bacterial pellet was resuspended in 20 mL of sterile normal saline to obtain viable stock cultures. The bacterial concentration was standardized to an optical density (OD) of 0.10 at 625 nm using a spectrophotometer, corresponding to approximately 1 x 108 CFU/mL (0.5 McFarland standard).

### 2.4.3 MIC determination

The minimum inhibitory concentration (MIC) was determined using the standard broth microdilution method according to Clinical and Laboratory Standards Institute (CLSI) guidelines (M07-A8) [31]. Silver nanoparticles synthesized using 1%, 3%, and 6% w/v ELE were tested. Serial two-fold dilutions of the AgNPs, ranging from 5 mg/mL to 0.156 mg/mL, were prepared in BHI broth. Each tube was inoculated with the standardized bacterial suspension approximately 1 × 108 CFU/mL. Controls consisted of inoculated broth without nanoparticles. All tubes were incubated at 37 °C for 24 h. The MIC was defined as the lowest concentration of AgNPs at which no visible bacterial growth was observed. Turbidity was visually assessed before and after incubation to confirm MIC values.

# 3.0 Results and Discussions

## 3.1 Phytochemical screening of the ELEs

Preliminary phytochemical screening of the ELE revealed the presence of the main classes of secondary metabolites (Table 1). The presence of phenols, flavonoids, tannins, saponins, and glycosides established its strong potential as a reducing and capping agent in the green synthesis of AgNPs. The abundant flavonoids and phenols are particularly significant, as these classes of compounds are consistently implicated in electron transfer processes that reduce Ag⁺ ions to metallic Ag⁰. Similar findings were reported by Khalil et al.[32], who demonstrated that phenolic-rich extracts from Phoenix dactylifera efficiently mediated AgNP formation with enhanced stability. In another study, Ahmed et al.[33] observed that tannins and flavonoids from Azadirachta indica leaf extract served dual roles as reducing and capping agents, yielding well-dispersed nanoparticles. Furthermore, Siddiqi et al. [34] highlighted that saponins and glycosides in Eucalyptus globulus contributed to nanoparticle stabilization, in line with the current results. This suggests that ELE's phenols, flavonoids, tannins, saponins, and glycoside metabolites operate synergistically to direct nanoparticle nucleation, growth, and stabilization during green synthesis.

Table 1: Phytochemicals qualitatively detected in the Eucalyptus leaf crude extract

| Secondary metabolites | Crude Extract | Inferences |
| --- | --- | --- |
| Alkaloids | - | Brown color |
| Phenols | +++ | Blue-black |
| Saponins | + | Persist foam |
| Flavanoids | ++ | Persist yellow precipitate |
| Terpenoids | - | Brown |
| Tannis | + | Black |
| Steroids test | - | Red-brown |
| Glycosides | + | Brown |
| Phlobatannis | - | Green |
| Antraquinones | _ | Blue |

*Key: (+++) = Abundance     (++) = Moderate        (+) = Present             (-) =Absent

## 3.2 Total Phenolics and Flavonoids

The phytochemical richness of the ELE was quantified in terms of total phenolic content (TPC) and total flavonoid content (TFC), as shown in Table 2. Both TPC and TFC increased with ELE concentration, rising from 31 mg GAE/g and 7 mg QAE/g at 1% to 78 mg GAE/g and 32 mg QAE/g at 6% w/v, respectively. This steady increase indicates that ELE provides abundant reducing and capping agents at higher concentrations, which directly influence nanoparticle nucleation and stabilization. Comparable findings in the literature show that Eucalyptus camaldulensis leaf extract generates stable silver nanoparticles due to its high phenolic content, which acts as both a reducing and stabilizing agent [35]. Similarly, biosynthesis using Eucalyptus globulus leaf extract demonstrated that flavonoid-rich fractions facilitated the production of uniformly dispersed, stable AgNPs with strong antimicrobial properties  [36,37].

Table 2: Total Phenolic and Flavonoid content in the ELE.

| ELE (% w/v) | TPC (mg GAE/g) | SD | TFC (mg QAE/g) | SD |
| --- | --- | --- | --- | --- |
| 1% | 31 | ±2 | 7 | ±1 |
| 3% | 43 | ±2 | 21 | ±2 |
| 6% | 78 | ±3 | 32 | ±2 |

## 3.4 UV-Vis analysis

The optical properties of the phytochemical-assisted green synthesis AgNPs examined using UV–Vis spectrophotometry are shown in Figure 2. A color transition from pale yellow to dark brown was observed upon the addition of ELE to silver nitrate solution, with increasing extract concentration the coloration intensified. The visible change corresponded to the excitation of surface plasmon resonance (SPR), confirming the reduction of Ag⁺ ions into Ag⁰ nanoparticles. Distinct SPR bands appeared at 420 for the 1% w/v, and 422nm for both 3% and 6% w/v ELE, consistent with the characteristic plasmonic response of silver nanoparticles of 400–500 nm range of the UV-Vis absorption spectrum, often centered around 400–430 nm [38]. The sharper and more intense peaks observed at 6% w/v ELE reflect a higher density of nanoparticles and improved stabilization due to the increased availability of reducing phytochemicals. These SPR positions agree well with prior reports of Eucalyptus-mediated AgNPs. For instance, [39] observed an SPR peak at approximately 423 nm when using Eucalyptus globulus extract, with peak intensity varying according to extract concentration. Similarly, a study on Eucalyptus camaldulensis extract reported a pronounced SPR band at 420 nm, confirming nanoparticle formation via green synthesis [40]. Moreover, the observed blue shift of the SPR relative to bulk silver is indicative of nanoscale dimensions and reduced particle size, a hallmark of nanoparticle behavior. This trend has been consistently reported across green synthesis aproaches using various plant extracts [41,42].

Figure 2. UV–Vis spectra of the phytochemical-assisted synthesis of AgNPs at 1% (a), 3%(b),  and 6% w/v (c) ELE.

## 3.5. FTIR Spectroscopy Analysis

FTIR spectroscopy was employed to establish the functional groups in the ELE responsible for reducing silver ions and stabilizing the synthesized nanoparticles. As shown in Figure 3, both the ELE and the phytochemical-assisted synthesized AgNPs displayed characteristic absorption bands. The broad peak around 3400 cm⁻¹ corresponds to O–H stretching vibrations of phenolic compounds and alcohols, which are key contributors to metal ion reduction. The band at around 2920 cm⁻¹ is attributed to C–H stretching from aliphatic hydrocarbons, while the strong absorption around 1630 cm⁻¹ can be assigned to C=O stretching vibrations of flavonoids, amides, and aromatic ketones, which could have participated in the reduction process. The band observed at 1400 cm⁻¹ is associated with O–H bending or C–N stretching, reflecting the presence of polyphenols. A distinct peak at 1100 cm⁻¹ corresponds to C–O stretching vibrations of alcohols, ethers, or glycosidic bonds, which might have played the role in the nanoparticle stabilization. Upon nanoparticle formation, shifts and reductions in peak intensities were evident, confirming the active involvement of these functional groups in Ag⁺ reduction and capping. This behavior was reported from different studies using plant extracts, for example, a study by Kaviya et al.[43], investigated the green synthesis of AgNPs using Citrus sinensis peel extract. FTIR analysis revealed characteristic peaks at approximately 3444, 2927, 2856, 1635, 1118, and 742 cm⁻¹, corresponding to O–H, C–H, and C=O stretching vibrations. These functional groups were identified as key contributors to the reduction of Ag⁺ ions and stabilization of the synthesized AgNPs [43,44].

Figure 3. FTIR spectra of the phytochemical-assisted synthesis of AgNPs at 1% (a), 3%(b), 6% w/v (c) ELE and pure ELE (d).

## 3.6 TEM Analysis

Figure 4 shows the morphological evolution of AgNPs synthesized using varying concentrations of ELE. At 1% w/v ELE (Figure 4a), particles appeared polydispersed and agglomerated, which could suggest insufficient phytochemical content for stabilization. At 3% w/v ELE (Figure 4b), the dispersion of the AgNPs improved, though minor clustering is seen. In Figure 4c, at 6% w/v ELE the AgNPs are polydispersed, spherical, and smaller in size, ranging from 2–28 nm with an average diameter of 12.90 ± 4.62 nm (Figure 4d). This concentration-dependent trend highlights that sufficient leaf extract concentrations provide abundant phytochemicals, especially phenolics and flavonoids that act as reducing and capping agents, enhancing nucleation and limiting growth, which results in smaller particle sizes. Similar findings were reported by [45], where AgNPs synthesized from Azadirachta indica extract exhibited particle sizes of 19–43 nm, while Cheng et al. [46] achieved well-dispersed AgNPs from mango peel extract with sizes ranging from 2.5–6.5 nm. These findings suggest that extract concentration directly influences phytochemical-mediated reduction and stabilization, making it a critical factor in controlling nanoparticle morphology during green synthesis.

Figure 4. TEM images of the phytochemical-assisted synthesis of AgNPs at 1% (a), 3% (b), and 6% w/v ELE (c) and TEM histogram (d).

## 3.7 XRD Analysis

Figure 5 shows the XRD diffraction patterns of AgNPs synthesized using ELE at 1%, 3%, and 6% concentrations compared to a standard reference. Prominent peaks at 2θ values at 38°, 44°, 64°, and 77° correspond to the (111), (200), (220), and (311) planes of face-centred cubic silver (JCPDS 04-0783). The sharp and well-defined peaks confirm high crystallinity. Average crystallite sizes, calculated using the Scherrer equation, were 9.42, 8.07, and 5.16 nm for 1%, 3%, and 6% w/v ELE, respectively. The reduction in particle size with higher extract concentration suggests stronger stabilization due to abundant phytochemicals. This observation aligns with the marked increase in TPC from 31–78 mg GAE/g and TFC from 7–32 mg QAE/g, which serve as key reducing and stabilizing agents in green synthesis. Phenolics and flavonoids donate electrons to Ag⁺ ions, enabling their rapid reduction to metallic Ag⁰, while simultaneously capping the particles to prevent uncontrolled growth. These findings are consistent with the FTIR results, where disappearance or shifting of O–H stretching, C=O stretching and aromatic C=C vibrations peaks after synthesis of the AgNPs (Figure 3).

Similar findings were reported on the use of Azadirachta indica leaf extract which produced crystalline AgNPs with face-centred cubic structure [47], and Camellia sinensis extract that yielded uniform nanoparticles with 4 nm AgNPs [48]. Likewise, Moringa oleifera and Spinacia oleracea leaf extract-mediated AgNPs showed smaller sizes at higher phytochemical loadings [49,50]. These findings affirm that ELE behaves consistently with other phytochemical-rich plants, yielding stable, nanosized, crystalline nanopaerticles.

Figure 5. XRD diffraction patterns of AgNPs reference spectrum (a), and phytochemical-assisted synthesis AgNPs at 1% (a), 3% (b), and 6% w/v (c) ELE.

## 3.8. Antibacterial Activity of the phytochemical-assisted green-synthesized AgNPs

Table 3 presents the antibacterial activity of silver nanoparticles synthesized with different concentrations of ELE against S. aureus and K. pneumoniae. The MIC decreased progressively with increasing extract concentration, reflecting enhanced antibacterial efficiency. For S. aureus, the MIC reduced from 0.200 mg/mL at 1% w/v AgNPs to 0.100 mg/mL at 6% w/v AgNPs. In the case of K. pneumoniae, the MIC dropped from 0.300 mg/mL at 1% w/v to 0.075 mg/mL at 6% w/v AgNPs. These values were consistently lower compared to the positive control, neomycin (1.500 mg/mL for S. aureus and 0.750 mg/mL for K. pneumoniae), confirming the superior antibacterial effectiveness of biosynthesized AgNPs.

Table 3. Antibacterial activity of phytochemical-assisted green-synthesized AgNPs using different concentrations of ELE and the control.

| Bacterial species | Concentrations (mg/mL) |  |  |  |
| --- | --- | --- | --- | --- |
|  | 1% w/v AgNPs | 3% w/v AgNPs | 6% w/v AgNPs | Neomycin |
| S. aureus | 0.200 | 0.150 | 0.100 | 1.500 |
| K. pneumoniae | 0.300 | 0.150 | 0.075 | 0.750 |

The enhanced antibacterial performance observed at higher extract concentrations may be linked to the formation of smaller AgNPs with larger surface-to-volume ratios. This structural feature increases the nanoparticles’ ability to anchor onto microbial membranes, causing protein denaturation, induction of oxidative stress, and ultimately cell death. Similar concentration-dependent antibacterial effects of phytochemical-mediated AgNPs have been documented in the literature. For instance, Chinnasamy et al. [49] reported that Azadirachta indica leaf extract-synthesized AgNPs exhibited strong bactericidal activity against E. coli and S. aureus, demonstrating a trend consistent with the present findings.

# Conclusion

This study demonstrated that phytochemical-assisted green synthesis of silver nanoparticles (AgNPs) using Eucalyptus globulus leaf extract is an effective, sustainable, and biocompatible approach for nanoparticle production. Structural characterization confirmed that phytochemicals, particularly phenolics and flavonoids, play a dual role as reducing and capping agents, thereby governing nanoparticle nucleation, growth, morphology, and stabilization. UV–Vis spectroscopy verified the formation of AgNPs through distinct surface plasmon resonance peaks, while FTIR, TEM, and XRD analyses revealed the presence of functional groups, spherical morphology, and crystalline face-centered cubic structures with size reduction at higher extract concentrations. Importantly, the concentration-dependent phytochemical availability led to enhanced nanoparticle dispersion, decreased crystallite size, and controlled morphology. Antimicrobial assays established that the biosynthesized AgNPs exhibit potent inhibitory activity against S. aureus and K. pneumoniae, surpassing standard antibiotics. These findings highlight the potential of Eucalyptus-mediated AgNPs for biomedical and pharmaceutical applications, emphasizing the importance of green nanotechnology in sustainable antimicrobial development. The biosynthesized AgNPs hold promise for practical applications such as wound dressings, antimicrobial surface coatings, and drug delivery systems. Future studies should focus on in vivo validation, cytotoxicity profiling, and long-term stability assessments to ensure safety and efficacy for clinical translation.

Disclaimer (Artificial intelligence)

Author(s) hereby declare that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc.) and text-to-image generators have been used during the writing or editing of this manuscript except Grammarly for language and grammar check.

# References

[1]	D.A. Anandhan, D.P.J. Bansod, Nanotechnology in the 21st Century: Innovation and Challenges, Addition Publishing House, 2025.

[2]	B. Tawiah, E.A. Ofori, S.C. George, Nanotechnology in Societal Development, in: S.C. George, B. Tawiah (Eds.), Nanotechnology in Societal Development, Springer Nature, Singapore, 2024: pp. 1–64. https://doi.org/10.1007/978-981-97-6184-5_1.

[3]	A. Dhaka, S. Chand Mali, S. Sharma, R. Trivedi, A review on biological synthesis of silver nanoparticles and their potential applications, Results in Chemistry 6 (2023) 101108. https://doi.org/10.1016/j.rechem.2023.101108.

[4]	R. Abbas, J. Luo, X. Qi, A. Naz, I.A. Khan, H. Liu, S. Yu, J. Wei, Silver Nanoparticles: Synthesis, Structure, Properties and Applications, Nanomaterials 14 (2024) 1425. https://doi.org/10.3390/nano14171425.

[5]	A.-C. Burdușel, O. Gherasim, A.M. Grumezescu, L. Mogoantă, A. Ficai, E. Andronescu, Biomedical Applications of Silver Nanoparticles: An Up-to-Date Overview, Nanomaterials 8 (2018) 681. https://doi.org/10.3390/nano8090681.

[6]	H. Jangid, S. Singh, P. Kashyap, A. Singh, G. Kumar, Advancing biomedical applications: an in-depth analysis of silver nanoparticles in antimicrobial, anticancer, and wound healing roles, Front. Pharmacol. 15 (2024). https://doi.org/10.3389/fphar.2024.1438227.

[7]	L. Xu, Y.-Y. Wang, J. Huang, C.-Y. Chen, Z.-X. Wang, H. Xie, Silver nanoparticles: Synthesis, medical applications and biosafety, Theranostics 10 (2020) 8996–9031. https://doi.org/10.7150/thno.45413.

[8]	A. Sati, T.N. Ranade, S.N. Mali, H.K. Ahmad Yasin, A. Pratap, Silver Nanoparticles (AgNPs): Comprehensive Insights into Bio/Synthesis, Key Influencing Factors, Multifaceted Applications, and Toxicity─A 2024 Update, ACS Omega 10 (2025) 7549–7582. https://doi.org/10.1021/acsomega.4c11045.

[9]	S.R. B., S.K. P., S. S., P. V., G. Rangasamy, D.-V.N. Vo, Innovative eco-friendly silver nanoparticles: various synthesis methods, characterization and prospective applications, Chemical Engineering Communications 212 (2025) 472–507. https://doi.org/10.1080/00986445.2024.2403117.

[10]	R. Kanwar, R. Fatima, R. Kanwar, M. Javid, U. Muhammad, Z. Ashraf, A. Khalid, A. Biological, Biological, physical and chemical synthesis of silver nanoparticles and their non-toxic bio-chemical application: A brief review physical and chemical synthesis of silver nanoparticles and their non-toxic bio-chemical application: A brief review. Pure and Applied Biology, 2022. https://doi.org/10.19045/bspab.2022.110042.

[11]	F. Kurul, B. Doruk, S.N. Topkaya, Principles of green chemistry: building a sustainable future, Discov. Chem. 2 (2025) 68. https://doi.org/10.1007/s44371-025-00152-9.

[12]	S.F. Ahmed, M. Mofijur, N. Rafa, A.T. Chowdhury, S. Chowdhury, M. Nahrin, A.B.M.S. Islam, H.C. Ong, Green approaches in synthesising nanomaterials for environmental nanobioremediation: Technological advancements, applications, benefits and challenges, Environmental Research 204 (2022) 111967. https://doi.org/10.1016/j.envres.2021.111967.

[13]	M. Thatyana, N.P. Dube, D. Kemboi, A.-L.E. Manicum, N.S. Mokgalaka-Fleischmann, J.V. Tembu, Advances in Phytonanotechnology: A Plant-Mediated Green Synthesis of Metal Nanoparticles Using Phyllanthus Plant Extracts and Their Antimicrobial and Anticancer Applications, Nanomaterials (Basel) 13 (2023) 2616. https://doi.org/10.3390/nano13192616.

[14]	E.M. Elias, G. Meganathan, M. Pappuswamy, Green synthesis, characterization, and biological applications of silver nanoparticles from Pachira glabra leaf extract, The Microbe 7 (2025) 100413. https://doi.org/10.1016/j.microb.2025.100413.

[15]	M. Fahim, A. Shahzaib, N. Nishat, A. Jahan, T.A. Bhat, A. Inam, Green synthesis of silver nanoparticles: A comprehensive review of methods, influencing factors, and applications, JCIS Open 16 (2024) 100125. https://doi.org/10.1016/j.jciso.2024.100125.

[16]	B. Cardoso, G. Nobrega, I.S. Afonso, J.E. Ribeiro, R.A. Lima, Sustainable green synthesis of metallic nanoparticle using plants and microorganisms: A review of biosynthesis methods, mechanisms, toxicity, and applications, Journal of Environmental Chemical Engineering 13 (2025) 116921. https://doi.org/10.1016/j.jece.2025.116921.

[17]	H.B. Habeeb Rahuman, R. Dhandapani, S. Narayanan, V. Palanivel, R. Paramasivam, R. Subbarayalu, S. Thangavelu, S. Muthupandian, Medicinal plants mediated the green synthesis of silver nanoparticles and their biomedical applications, IET Nanobiotechnol 16 (2022) 115–144. https://doi.org/10.1049/nbt2.12078.

[18]	C.K. Ezeh, C.N. Eze, M.U.E. Dibua, S.C. Emencheta, A review on Azadirachta indica (neem) plant mediated biosynthesis, characterisation and antimicrobial activity of silver nanoparticles, International Journal of Biomedical Nanoscience and Nanotechnology 5 (2024) 15–36. https://doi.org/10.1504/IJBNN.2024.139351.

[19]	H. Khan, M. Kataria, M.A. Khan, Antimicrobial Efficacy of Neem Extract–Stabilized Metal Nanoparticles, in: Nanotechnological Approaches in Food Microbiology, CRC Press, 2020.

[20]	S. Shahzadi, S. Fatima, Q. ul Ain, Z. Shafiq, M.R.S. Ashraf Janjua, A review on green synthesis of silver nanoparticles (SNPs) using plant extracts: a multifaceted approach in photocatalysis, environmental remediation, and biomedicine, RSC Advances 15 (2025) 3858–3903. https://doi.org/10.1039/D4RA07519F.

[21]	G. Singhal, R. Bhavesh, K. Kasariya, A.R. Sharma, R.P. Singh, Biosynthesis of silver nanoparticles using Ocimum sanctum (Tulsi) leaf extract and screening its antimicrobial activity, J Nanopart Res 13 (2011) 2981–2988. https://doi.org/10.1007/s11051-010-0193-y.

[22]	S. Ferdous, G.S. Rahman, J. Rayhan, M.Z. Hossain, M.H. Rahman, A. Khan, M.S. Islam, Green Synthesis of Silver Nanoparticles Using Moringa oleifera Leaf Extract: Antibacterial Efficacy and Sustainable Nanotechnology, Biosensors and Nanotheranostics 3 (2024) 1–8. https://doi.org/10.25163/biosensors.319971.

[23]	S. Nile, Y.S. Keum, Chemical composition, antioxidant, anti-inflammatory and antitumor activities of eucalyptus globulus labill., Indian Journal of Experimental Biology 56 (2018) 734–742.

[24]	Surbhi, A. Kumar, S. Singh, P. Kumari, P. Rasane, Eucalyptus: phytochemical composition, extraction methods and food and medicinal applications, Advances in Traditional Medicine 23 (2021). https://doi.org/10.1007/s13596-021-00582-7.

[25]	M.U. Sadiq, A. Shah, A. Haleem, S.M. Shah, I. Shah, Eucalyptus globulus Mediated Green Synthesis of Environmentally Benign Metal Based Nanostructures: A Review, Nanomaterials 13 (2023) 2019. https://doi.org/10.3390/nano13132019.

[26]	K. Ali, B. Ahmed, S. Dwivedi, Q. Saquib, A. Al-Khedhairy, J. Musarrat, Microwave Accelerated Green Synthesis of Stable Silver Nanoparticles with Eucalyptus globulus Leaf Extract and Their Antibacterial and Antibiofilm Activity on Clinical Isolates, PLoS ONE (2015).

[27]	J. Shaikh, M. Patil, Qualitative tests for preliminary phytochemical screening: An overview, International Journal of Chemical Studies 8 (2020) 603–608. https://doi.org/10.22271/chemi.2020.v8.i2i.8834.

[28]	E.A. Ainsworth, K.M. Gillespie, Estimation of total phenolic content and other oxidation substrates in plant tissues using Folin–Ciocalteu reagent, Nat Protoc 2 (2007) 875–877. https://doi.org/10.1038/nprot.2007.102.

[29]	R.M. Lamuela-Raventós, Folin–Ciocalteu method for the measurement of total phenolic content and antioxidant capacity, in: Measurement of Antioxidant Activity & Capacity, John Wiley & Sons, Ltd, 2018: pp. 107–115. https://doi.org/10.1002/9781119135388.ch6.

[30]	A.M. Shraim, T.A. Ahmed, M.M. Rahman, Y.M. Hijji, Determination of total flavonoid content by aluminum chloride assay: A critical evaluation, LWT 150 (2021) 111932. https://doi.org/10.1016/j.lwt.2021.111932.

[31]	P. Parvekar, J. Palaskar, S. Metgud, R. Maria, S. Dutta, The minimum inhibitory concentration (MIC) and minimum bactericidal concentration (MBC) of silver nanoparticles against Staphylococcus aureus, Biomater Investig Dent 7 (2020) 105–109. https://doi.org/10.1080/26415275.2020.1796674.

[32]	M.M.H. Khalil, E.H. Ismail, K.Z. El-Baghdady, D. Mohamed, Green synthesis of silver nanoparticles using olive leaf extract and its antibacterial activity, Arabian Journal of Chemistry 7 (2014) 1131–1139. https://doi.org/10.1016/j.arabjc.2013.04.007.

[33]	S. Ahmed, Saifullah, M. Ahmad, B.L. Swami, S. Ikram, Green synthesis of silver nanoparticles using Azadirachta indica aqueous leaf extract, Journal of Radiation Research and Applied Sciences 9 (2016) 1–7. https://doi.org/10.1016/j.jrras.2015.06.006.

[34]	K.S. Siddiqi, A. Husen, R.A.K. Rao, A review on biosynthesis of silver nanoparticles and their biocidal properties, J Nanobiotechnology 16 (2018) 14. https://doi.org/10.1186/s12951-018-0334-5.

[35]	I. Alghoraibia, C. Soukkarieh, R. Zein, A. Alahmad, J.-G. Walter, M. Daghestani, Aqueous Extract of Eucalyptus Camaldulensis Leaves as a Reducing and Capping Agent in Green Synthesis of Silver Nanoparticles, Http://Www.Eurekaselect.Com (2019). https://www.eurekaselect.com/article/99199 (accessed August 27, 2025).

[36]	M. Balamurugan, S. Saravanan, Green Synthesis of Silver Nanoparticles by using Eucalyptus Globulus Leaf Extract, J. Inst. Eng. India Ser. A 98 (2017) 461–467. https://doi.org/10.1007/s40030-017-0236-9.

[37]	Y. Mo, Y. Tang, S. Wang, J. Lin, H. Zhang, D. Luo, Green synthesis of silver nanoparticles using eucalyptus leaf extract, Materials Letters 144 (2015) 165–167. https://doi.org/10.1016/j.matlet.2015.01.004.

[38]	W. Zhu, Q. Hu, Q. Wang, J. Yan, Determination of trace rutin based on the surface plasmon resonance absorption of silver nanoparticles, Anal. Methods 6 (2014) 2751–2755. https://doi.org/10.1039/C3AY41909F.

[39]	A.A. Subhani, M. Irshad, S. Ali, M. Jawad, M.F. Akhtar, M. Summer, UV-spectrophotometric Optimization of Temperature, pH, Concentration and Time for Eucalyptus Globulus Capped Silver Nanoparticles Synthesis, their Characterization and Evaluation of Biological Applications, J Fluoresc 34 (2024) 655–666. https://doi.org/10.1007/s10895-023-03260-w.

[40]	Y. ÇETİNTAŞ, S. Nadeem, E. SAKALLI, E. ELİUZ, M. ÖZLER, GREEN SYNTHESIS, ANTIMICROBIAL AND ANTICANCER ACTIVITIES OF AgNPs PREPARED FROM THE LEAF EXTRACT OF Eucalyptus camaldulensis, Mugla Journal of Science and Technology 6 (2020). https://doi.org/10.22531/muglajsci.714696.

[41]	H. Munir, A. Mumtaz, R. Rashid, J. Najeeb, M.T. Zubair, S. Munir, M. Bilal, H. Cheng, Eucalyptus camaldulensis gum as a green matrix to fabrication of zinc and silver nanoparticles: Characterization and novel prospects as antimicrobial and dye-degrading agents, Journal of Materials Research and Technology 9 (2020) 15513–15524. https://doi.org/10.1016/j.jmrt.2020.11.026.

[42]	T. Bashir, M.Z. Qureshi, PHYTOSYNTHESIS OF SILVER NANOPARTICLES USING E. CAMALDULENSIS LEAF EXTRACT AND THEIR CHARACTERIZATION, Journal of the Chilean Chemical Society 60 (2015) 2861–2863. https://doi.org/10.4067/S0717-97072015000100019.

[43]	S. Kaviya, J. Santhanalakshmi, B. Viswanathan, J. Muthumary, K. Srinivasan, Biosynthesis of silver nanoparticles using citrus sinensis peel extract and its antibacterial activity, Spectrochim Acta A Mol Biomol Spectrosc 79 (2011) 594–598. https://doi.org/10.1016/j.saa.2011.03.040.

[44]	K.N. Nahar, Md.H. Rahaman, G.M.A. Khan, Md.K. Islam, S.Md. Al-Reza, Green synthesis of silver nanoparticles from Citrus sinensis peel extract and its antibacterial potential, Asain J. Green Chem. 5 (2021). https://doi.org/10.22034/ajgc.2021.113966.

[45]	K. K, J. S, Silver nanoparticles synthesized using leaf extract of Azadirachta indica exhibit enhanced antimicrobial efficacy than the chemically synthesized nanoparticles: A comparative study, Science Progress 104 (2021). https://doi.org/10.1177/00368504211012159.

[46]	J. Cheng, X. Lin, X. Wu, Q. Liu, S. Wan, Y. Zhang, Preparation of a multifunctional silver nanoparticles polylactic acid food packaging film using mango peel extract, Int J Biol Macromol 188 (2021) 678–688. https://doi.org/10.1016/j.ijbiomac.2021.07.161.

[47]	B. Avinash, R. Venu, T.N.V.K.V. Prasad, M. Alpha Raj, K. Srinivasa Rao, C. Srilatha, Synthesis and characterisation of neem leaf extract, 2, 3‐dehydrosalanol and quercetin dihydrate mediated silver nano particles for therapeutic applications, IET Nanobiotechnol 11 (2016) 383–389. https://doi.org/10.1049/iet-nbt.2016.0095.

[48]	Y.Y. Loo, B.W. Chieng, M. Nishibuchi, S. Radu, Synthesis of silver nanoparticles by using tea leaf extract from Camellia sinensis, Int J Nanomedicine 7 (2012) 4263–4267. https://doi.org/10.2147/IJN.S33344.

[49]	H. Perumalsamy, S.R. Balusamy, J. Sukweenadhi, S. Nag, D. MubarakAli, M. El-Agamy Farh, H. Vijay, S. Rahimi, A comprehensive review on Moringa oleifera nanoparticles: importance of polyphenols in nanoparticle synthesis, nanoparticle efficacy and their applications, Journal of Nanobiotechnology 22 (2024) 71. https://doi.org/10.1186/s12951-024-02332-8.

[50]	T. Akpobolokemi, E. Chung, R. Teresa Martinez-Nunez, G. Ren, B.T.R. Abraham, A. Griffiths, Influence of Spinacia oleracea leaf extract concentration on silver nanoparticle formation and evaluation of antimicrobial properties, RSC Pharmaceutics 2 (2025) 353–368. https://doi.org/10.1039/D4PM00302K.