# Review of Applications and Challenges Facing

# use of Nanofluids

.

# ABSTRACT

Fluids containing nanoparticle suspensions features significantly in heat transfer applications. This is attributed to their superior thermophysical properties compared to the conventional fluids. The thermophysical properties of nanofluids that makes them attractive for use in various fields include; enhanced thermal conductivity, convective heat transfer coefficient, viscosity, density, heat capacity, thermal diffusivity, emissivity and optical absorption. The current paper reviews the current trends in the application of nanofluids in various fields such as nanomedicine, renewable energy applications, automotive applications, electronic cooling applications, heating buildings, space and defense and in microbial fuel cell. The paper also explores the challenges associated with the use of nanofluids such as long term stability of nanoparticle dispersion, increased pressure drop and pumping power, toxicity and environmental implications associated with the use of nanofluids.

Key words: Developments, Applications, Nanofluids, Recent

# Introduction

“Nanofluids are embryonic fluids enriched with ultrafine solid nanoparticles. The nanoparticles sizes range from (1 − 100𝑛𝑚) making nanofluids behave more like a single phase fluid rather than a solid-liquid mixture. The nanoparticles used in the synthesis of nanofluids consist of chemically stable metals (Al, Cu, Ag , Au, Fe), nonmetals(graphite, carbon nanotubes), oxides ceramics (Al2O3, CuO, TiO2, SiO2), carbides(𝑆𝑖𝐶), nitrides (AIN, SIN), layered (Al+, Al2O3, Cu + C)PCM, and functionalized nanoparticles. The host fluid used in the preparation of nanofluids are usually a conductive fluid, such as water, (or other coolants), oil (and other lubricants), polymer solutions, bio fluids and other common fluids, such as paraffin. Nanofluids were first engineered by” (Choi & Eastman, 1995) of the Argonne national laboratory, USA in 1995. Nanofluids show advanced thermal-physical properties such as thermal conductivity, convective heat transfer coefficient, viscosity, density, heat capacity, thermal diffusivity, emissivity and optical absorption in comparison to the conventional base fluids (Murshed, 2025; Razzaq et al., 2025). Nanofluids can be classified as Metallic Nanofluids i.e. nanofluids prepared by dispersing nanoparticles made from chemically stable metals such as (Al, Cu, Fe, Zn, Ni, Si, Ti, Au and Ag) into the host fluid, Non-Metallic Nanofluids, i.e. Nanofluids prepared by suspending nanoparticles made from nonmetals into the host fluid. The nonmetals used include metal oxides (𝐶𝑢𝑂, Al2O3, SiC, 𝑍𝑛𝑂, TiO2 ), Semiconductors such as (TiO2) and Carbon Nanotubes (SWCNT, MWCNT, and DWCNT ), and composites materials such as nanoparticles core polymer shell composites, and Hybrid nanofluids (i.e. nanofluids dispersed with two or more different types of nanoparticles). Nanofluids owing to their advanced thermophysical properties continues to attract a lot of attention due to their possible use in numerous fields.

# Applications of Nanofluids

Nanofluids can be used in various heat transfer applications due to their superior thermophysical properties compared to those of conventional fluids. The following are some of the applications of nanofluids:

# Nanomedicine

Nanomedicine involves harnessing the power of nanotechnology in detection, diagnosis and treatment of diseases. The use of Nanotechnology in the diagnosis and treatment of cancer as an alternative to traditional methods of cancer treatment (chemotherapy, radiotherapy, and surgery) looks promising. Nanotechnology has been successfully deployed in targeted drug delivery, molecular (tumor) imaging, targeted therapy, phototherapy, gene therapy and Radiofrequency ablation of cancerous cells. With regards to nanomedicine the following areas are discussed in detail; Nanoparticle-based cancer imaging, Nano drug delivery and Nanocryosurgery.

# Nanoparticle-Based Cancer Imaging

Tumor imaging by deploying nanoparticles helps in early detection of cancerous cells (Jin et al., 2020) . The materials used in generating Nanoparticle imaging probe should be biodegradable, of low toxicity, be easily excreted from the body system and be able to provide strong imaging signal. “Nanoparticles used to create imaging probes for cancer treatment possesses unique properties such as unique optical, magnetic and chemical properties. This results in imaging probes with increased signal density, signal amplification and quantification, improved contrast, and controlled biodistribution”(Chapman et al., 2013). 𝜋 −Conjugated nanoprobes are used in brain tumor-related studies, due to their excellent electronic structure, optical properties and photothermal therapy to deactivate tumor cells by elevating temperature (Ma et al., 2021; Sun et al., 2023). The nanoparticles currently being used to create imaging probes include gold nanoparticles, iron oxide nanoparticles, lipid nanoparticles, silica- based nanoparticles, polymeric nanoparticles and Quantum dots.

# Nanocryosurgery

Nanocryosurgery is a medical procedure that incorporates nanoparticles in freezing of tumor or cancerous cells. The target cells are intentionally loaded with nanoparticles of high thermal conductivity to speed up the freezing process. According to (Ammar et al., 2025; Hou et al., 2018; B. Wang et al., 2024) intentionally loading of target tissues with nanoparticles of superior thermal conductivity results in the overall decrease of the final temperature of the tumor resulting in maximum freezing rate. The nanoparticles deployed in the nanocryosurgery should be nontoxic, biodegradable and have few side-effects on the human body (Di et al., 2012) . The therapy is becoming popular in treatment and management of cancer due to its clinical advantages as opposed to the traditional methods. Diamond, magnetite (Fe3O4) and magnesium oxide (MgO) nanoparticles are preferred in enhancing freezing due to their good biological compatibility.

# Nanodrug delivery

“Nanodrug delivery involves use of nanoparticle drug carriers for targeted drug delivery to the affected tissues, improving drug efficacy and minimizing the related side effects. The conventional routes currently being used for drug delivery include; oral, buccal, rectal, subcutaneous, intranasal, intramuscular, intravenous, pulmonary and transdermal which are often characterized by limitations such as instability, risk of displacement, uncontrolled release of drug, side effects such as irritation and pain, slow absorption and enzymatic deterioration. The use of magnetic nanoparticles” (Graham et al., 2025; Rarokar et al., 2024; Riaz et al., 2025) as nanocarriers allows doctors to precisely deliver high local doses of drugs or radiation to the affected tissue without damaging neighboring healthy tissues. This magnetic drug delivery overcomes the major drawback of the traditional methods such as chemotherapy which is often characterized by the inability to precisely deliver and concentrate drugs to the affected tissues and organs resulting in free circulation of drugs in the bloodstream which affects other healthy tissues and organs. “Nanodrug delivery trials are being conducted in the field of cancer where magnetic nanofluids (ferrofluids) are being used

to guide the cancer drugs up the bloodstream to the tumors with the help of magnets. The nanocarriers currently in use include; solid nanoparticles, liposomes, dendrimers, polymeric nanoparticles, polymeric micelles, virus like nanoparticles, carbon nanotubes and mesoporous silica nanoparticles” (Sultana et al., 2022) with the following drug delivery systems currently in use; nucleic acid-based drug delivery system, cell-based drug delivery system, self-nano emulsifying drug delivery system, self-micro emulsifying drug delivery system, chemical and physical stimuli-based drug delivery system, nanoneedles, patches, ultrasound drug delivery and microchip technology.

Figure 1: Biomedical application of Nanofluids (Image source: Intechopen.com)

# Renewable energy applications

- Geothermal Power Extraction

During the drilling process to extract thermal or heat energy from the earth’s crust where the drilling lengths usually vary from (5 − 10𝑘𝑚) and high temperatures of between (500℃ − 1000℃) are involved, the major limiting factor becomes the thermal limitations of the drilling tools, sensory devices and pipes. Nanofluids due to their high thermal conductivity (fluid superconductors) plays a vital role in extraction of geothermal energy. They are deployed in geothermal well construction to cool down pipes, machineries and other equipment working under extreme high temperatures and

friction conditions, in geothermal reservoir characterization, scaling and corrosion prevention and resource recovery (Meng et al., 2025). The use of nanofluids during drilling permits sensors and other electronic devices to operate under high temperature allowing access to deeper and hotter regions which boosts the amount of thermal energy extracted from the ground.

Figure 2: Various applications of nanotechnology in geothermal energy systems (Image source Canstrat Inc. (2024), Kurita Europe (2024))

# Solar Energy Absorption.

Solar energy being renewable and environmental friendly, its use in most engineering applications that require heating and cooling is becoming popular. These applications range from heating living spaces, solar electric power generation, and solar cookers to solar water-heating systems among others. The conventional direct absorption solar collector used in various applications such as water heating is a well-established technology but whose operation is always limited by the working fluid used. This technology when combined with nanofluids as the working fluid, the efficiency of these collectors can be enhanced (Alcázar et al., 2025; Hamzat et al., 2022; Zahra Haeri et al., 2025). The experimental study by (Eriksen et al., 2024) on direct absorption solar collector incorporating carbon black nanofluid for solar energy harvesting reported a 42%   thermal enhancement at 0.01𝑤𝑡. %  nanoparticle

concentration in reference to distilled water. (Nguyen et al., 2023) investigation on direct absorption solar collector utilizing carbon black nanofluid as the working fluid noted a 102% thermal enhancement when compared to pure water. (Sani et al., 2010) investigating optical and thermal properties of nanofluids containing aqueous suspensions of single-wall carbon nanohorns observed improved optical properties which led to considerable higher sunlight absorption.

Figure 3: Nanofluid use as a heat transfer fluid in solar thermal collectors (Image source: link.springer.com)

# Automotive Applications

Nanofluids due to their superior thermophysical, rheological and tribological properties they are increasingly being used in automobiles as automatic transmission fluids, in engine oils, as nanolubricants and being incorporated in the automobile radiators as coolants.

# Nanofluid coolant

“The use of nanofluids as coolants would allow for smaller size and better positioning of the radiators” (Ramadhan et al., 2020; Subhedar et al., 2024). “The addition of nanoparticles to the standard engine coolant improves automotive and heavy-duty engine cooling rates” (Hajiakbari et al., 2024) . “This removes engine heat with a reduced size coolant system. Smaller coolant systems results in smaller and lighter radiators which enhances fuel economy. Improved cooling rates can also be used to remove

more heat from higher horsepower engines with the same size of coolant system. In trucks with large radiators positioned in front of the engines to maximize on the cooling effect of the oncoming air, about 65% of the total energy output from the truck is used in overcoming the aerodynamic drag caused by the oncoming air and this result in increased fuel consumption” (McCallen et al., 2007).

# Friction Reduction (Lubricants)

“In automotive lubrication applications, surface-modified nanoparticles stably dispersed in engine oil have effective load-carrying capacity, good extreme pressure and friction reducing properties”. (Alnajjar et al., 2025) investigating use of carbon nanotubes as lubricant additive for automotive use reported enhancement in tribological, thermophysical and rheological properties compared to the bare sample of the lubricant. They reported reduction in wear and friction, enhanced lubrication performance and enhanced low-temperature performance. (Okello et al., 2021) examining the performance of engine oil-based hybrid nanolubricants reported least coefficient of skin friction in engine oil dispersed with (𝑀𝑊𝐶𝑁𝑇𝑠 − 𝑇𝑖𝑂2) hybrid nanoadditive making it suitable for automotive application. (Zhou et al., 2000) investigating tribological behavior of Cu nanoparticles in oil on a four-ball machine observed that Cu nanoparticles as oil additive had better friction-reduction and antiwear properties compared to Zinc dithiophosphate especially at high applied load.

# Nanofluids as Vehicular Brake Fluids

“During braking in motor vehicles, the vehicle’s kinetic energy is dispersed to heat energy which is transmitted throughout the brake fluid in the hydraulic braking system” (Popa et al., 2010). “With high demand in properties of brake oils, Aluminium- oxide and copper- oxide based brake nanofluids which have higher boiling point, higher viscosity and higher thermal conductivity compared to traditional brake fluid were manufactured using Plasma charging arc system and Arc-submerged nanoparticle synthesis systems respectively” (M. J. Kao et al., 2007; M.-J. Kao et al., 2007).This

enhanced Thermophysical properties of nanofluid brake oil minimizes occurrence of vapor-lock and enhances safety while driving.

# Electronic Applications

“In advanced electronic devices which are usually occasioned with high density microchips and the need to design more compact electronic devices, heat dissipation from such devices becomes a major challenge. This is because of high levels of heat generation and the reduced surface area for heat removal. A reliable thermal management system is therefore crucial for smooth operation of these devices. Two approaches can be used to achieve this, one is to find an optimum geometry of cooling devices and the other is to increase heat transfer capacity. Nanofluids due to their enhanced thermal conductivity and increased heat transfer coefficient they can be used for liquid cooling of computer processors” (Nanan Kwanchai et al., 2024; Okello et al., 2020). A new cooler combined microchannel heat sink developed by (Jang & Choi, 2006) with nanofluids produced a higher cooling performance compared to using pure water as the working medium. This is because nanofluids reduce thermal resistance as well as temperature difference between heated microchannel wall and coolant. Investigations by (Rohaizan et al., 2023) on liquid cooling using nanocellulose resulted in better thermal conductivity enhancement compared to the base fluid signaling the potential use of nanocoolant in a CPU cooling system.

Figure 4: Nanofluids in microchannel heat sink

(Image source: ScienceDirect.com)

# Other Applications of Nanofluids

    - Heating Buildings and Reducing Pollution

“In cold regions nanofluids can be used in heating buildings. A mixture of ethylene or propylene glycol with water mixed in different proportions is commonly used as a heat transfer fluid. Study by” (Alqarni et al., 2023) on shell and tube heat exchanger filled with hybrid nanofluid noted improvement in heat exchangers energy efficiency as a result of the use of nanofluid. (D. Wang et al., 2023) in their study reported a 126% increment in thermal performance of the heat exchanger which was attributed to the use nanofluid. This resulted in decrease in environmental damage, energy consumption and emissions. Investigations on shell and tube heat exchanger incorporating (𝑐𝑜𝑝𝑝𝑒𝑟 (𝑖𝑖)𝑜𝑥𝑖𝑑𝑒/𝑤𝑎𝑡𝑒𝑟) nanofluid by (Cruz et al., 2022) revealed a 48% enhancement in heat transfer which was attributed to the presence of nanofluid. The use of nanofluids in heat exchangers has shown the ability to reduce volumetric and mass flow rates, resulting in an overall pumping power savings. Nanofluids necessitate smaller heating systems capable of delivering same amount of heat energy as larger heating systems and they are less expensive. Smaller heating systems use less power and the heat transfer unit has also less liquid and therefore the material waste to be discarded at the end of its life cycle is small. This in long turn lowers pollution caused to the environment.

# Space and Defense

“Nanofluids have a wide application in space and defense fields, where power density is very high and the components are required to be small and weightless. Due to the restriction of space, energy, and weight in space station and aircraft there is need for high efficient cooling system with smaller size” (Bacha et al., 2024). This ultrahigh- heat flux cooling systems can be achieved by incorporating nanofluids (Di Lorenzo et al., 2025; Ungar & Erickson, 2011) . In military a number of devices and systems require high-heat flux cooling to the level of tens of MW/m2 for reliable operations.

Nanofluids with high critical heat fluxes have the ability to provide the required cooling in such systems and other systems such as military vehicles, submarines and high-power laser diodes.

# Nanofluids-Based Microbial Fuel Cell

“Microbial fuel cells (MFC) uses energy found in carbohydrates, proteins and other energy-rich natural products to produce electrical power. Their excellent performance depends on electrodes and electron mediator used”. (Sharma et al., 2008) constructed a novel MFC using novel electron mediators (nanofluids prepared by dispersing nanocrystalline platinum anchored CNTs in water) and CNT-based electrodes. They compared the performance of this E. coli-based MFC (CNT-based nanofluid & CNT- based electrodes) to plain graphite electrode-based MFC and CNT-based electrode showed as high as ~6-fold increase in power density compared to graphite electrode. This result shows the ability of noble metal nanoparticles dispersed on CNT-based MFC for generation of high energies from simple bacteria like E. coli.

# Challenges in the Application of Nanofluids

The use of nanofluids in heat transfer applications still faces numerous setbacks. The challenges associated with the use of nanofluid are centred on the long term stability of the nanoparticle dispersion, increased pressure drop and pumping power, lower specific heat capacity and toxicity and environmental pollution.

# Long term Stability of Nanoparticle Dispersion

Preparation of homogeneous nanofluid suspension remains a challenge due to aggregation (agglomeration) of nanoparticles (Loza et al., 2019; Rezvani et al., 2025). The forces impacting the nanofluid include Van der Waal attractive force, gravitational force, buoyancy force and electrostatic repulsive force. The Van der Waal attractive force and gravitational force suppresses the stability of any colloidal suspension. The other factors contributing to the destabilization of the nanofluid include particle size, sonication time, type of nanoparticles and the base fluid, and thermophoresis (Das et

al., 2024; Rahman et al., 2024). The stabilization techniques employed include ultrasonic agitation, surface modification techniques, pH control and addition of surfactants. Introducing surfactants enhances stability of the nanofluid by reducing the surface tension between the nanoparticles and the host fluid resulting in less agglomeration.

# Increased pressure drop and pumping power

The efficiency of the nanofluid as a coolant is hindered by the increased pressure drop during the flow brought about by high viscosity and high density of the nanofluid compared to the base fluid. Increased pressure drop impedes nanofluid use as a coolant due to cost incurred in pumping the nanofluid to sustain continuous flow (Awais et al., 2021; Khashaei et al., 2024; Shiravi et al., 2020).

# Lower Specific heat capacity

Some studies have reported low specific heat capacity of the nanofluid in comparison to the base fluid. Investigation by (Namburu et al., 2009) revealed low specific heat capacity  in  (𝐶𝑢𝑂/𝑒𝑡ℎ𝑦𝑙𝑒𝑛𝑒 𝑔𝑙𝑦𝑐𝑜𝑙), (𝑆𝑖𝑂2/𝑒𝑡ℎ𝑦𝑙𝑒𝑛𝑒 𝑔𝑙𝑦𝑐𝑜𝑙),  and  (𝐴𝑙2𝑂3/

𝑒𝑡ℎ𝑦𝑙𝑒𝑛𝑒 𝑔𝑙𝑦𝑐𝑜𝑙) nanofluids in comparison to the base fluid. This limits their use as

coolants in heat transfer applications since a good coolant should be of very high specific heat capacity.

# Toxicity and Environmental Implications

Nanofluid use though attractive due to their advanced thermophysical properties, they pose a significant risk to both the environment and the humans attributed to the increased exposure to the nanoparticles through inhalation, ingestion or dermal contact. Nanoparticle use for medical purposes if not well handled can lead to cardiovascular diseases (Kim et al., 2025). Nanoparticles circulating in the bloodstream can induce cellular death, oxidative stress, endothelial dysfunction, hyper permeability, procoagulant activity and general inflammation of the cardiovascular system (Gerogianni et al., 2023; Yousef et al., 2019, 2022). Nanoparticle waste

released into the aquatic environment pose a serious threat to aquatic life. Nanoparticle contaminants have resulted in organ failure in fish (Lekamge et al., 2020; López- Barrera et al., 2021). The consumption of nano contaminated fish species by humans may result in long term health risks.

# Conclusion

This article has reviewed the applications and challenges associated with the use of nanofluids which are emerging as a new breed of heat transfer fluids. These fluids possess advanced thermophysical properties making them suitable as coolants across various applications.

Abbreviations

CNT- Carbon Nanotube

SWCNT-Single-Walled Carbon Nanotube MWCNT-Multi-Walled Carbon Nanotube DWCNT-Double-Walled Carbon Nanotube MFC- Microbial Fuel Cell

DASC- Direct Absorption Solar Collector CPU- Central Processing Unit

# Disclaimer (Artificial Intelligence)

Authors hereby declare that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc) and text-to-image generators have been used during writing or editing of this manuscript.

# Competing Interests

Authors have declared that no competing interests exist.

# REFERENCES

Alcázar, H. E., Lanza, F. A., Aguilar, L. A., Patiño, L. E., Carpio, M. A., Neira Villena,

J. E., & Alcázar, L. O. (2025). The plasmonic effect of silver nanofluids in the solar energy harvesting. Materials Research Express, 12(4), 045002.

Alnajjar, D., Elsoudy, S., & Farrag, N. M. (2025). Carbon Nanotube-Enhanced Nanolubricants: Stability and Performance Improvements for Automotive Use. Egyptian Journal of Chemistry, 68(7), 379–385.

Alqarni, M. M., Ibrahim, M., Assiri, T. A., Saeed, T., Mousa, A. A. A., & Ali, V. (2023). Two-phase simulation of a shell and tube heat exchanger filled with hybrid nanofluid. Engineering Analysis with Boundary Elements, 146, 80–88.

Ammar, M. M., Ali, R., Abd Elaziz, N. A., Habib, H., Abbas, F. M., Yassin, M. T., Maniah, K., & Abdelaziz, R. (2025). Nanotechnology in oncology: Advances in biosynthesis, drug delivery, and theranostics. Discover Oncology, 16(1), 1172.

Awais, M., Ullah, N., Ahmad, J., Sikandar, F., Ehsan, M. M., Salehin, S., & Bhuiyan,

A. A. (2021). Heat transfer and pressure drop performance of Nanofluid: A state-of- the-art review. International Journal of Thermofluids, 9, 100065.

Bacha, H. B., Ullah, N., Hamid, A., & Shah, N. A. (2024). A comprehensive review on nanofluids: Synthesis, cutting-edge applications, and future prospects. International Journal of Thermofluids, 22, 100595.

Chapman, S., Dobrovolskaia, M., Farahani, K., Goodwin, A., Joshi, A., Lee, H., Meade, T., Pomper, M., Ptak, K., Rao, J., Singh, R., Sridhar, S., Stern, S., Wang, A., Weaver, J. B., Woloschak, G., & Yang, L. (2013). Nanoparticles for cancer imaging: The good, the bad, and the promise. Nano Today, 8(5), 454– 460.

Choi, S. U. S., & Eastman, J. A. (1995). Enhancing Thermal Conductivity of Fluids with Nanoparticles, Development and Application of Non-Newtonian Flows. ASME Journal of Heat Transfer, 66, 99–105.

Cruz, P. A. D., Yamat, E.-J. E., Nuqui, J. P. E., & Soriano, A. N. (2022). Computational Fluid Dynamics (CFD) analysis of the heat transfer and fluid flow of copper (II) oxide-water nanofluid in a shell and tube heat exchanger. Digital Chemical Engineering, 3, 100014.

Das, P. K., Santra, A. K., Ganguly, R., Dash, S. K., Muthusamy, S., Sha, M., & Sadasivuni, K. K. (2024). An extensive review of preparation, stabilization, and application of single and hybrid nanofluids. Journal of Thermal Analysis and Calorimetry, 149(17), 9523–9557.

Di, D.-R., He, Z.-Z., Sun, Z.-Q., & Liu, J. (2012). A new nano-cryosurgical modality for tumor treatment using biodegradable MgO nanoparticles. Nanomedicine: Nanotechnology, Biology and Medicine, 8(8), 1233–1241.

Di Lorenzo, G., Romano, D. G., Carozza, A., & Pagano, A. (2025). Nanofluids as Coolants to Improve the Thermal Management System of a High-Power Aircraft Electric Motor. Electronics, 14(5), 911.

Eriksen, A. B., Kosinski, P., Balakin, B. V., & Kosinska, A. (2024). Experimental study of a direct absorption solar collector with stationary nanofluid. Energy Conversion and Management: X, 23, 100683.

Gerogianni, A., Bal, M., Mohlin, C., Woodruff, T. M., Lambris, J. D., Mollnes, T. E., Sjöström, D. J., & Nilsson, P. H. (2023). In vitro evaluation of iron oxide nanoparticle-induced thromboinflammatory response using a combined human whole blood and endothelial cell model. Frontiers in Immunology, 14, 1101387.

Graham, W., Torbett-Dougherty, M., Islam, A., Soleimani, S., Bruce-Tagoe, T. A., & Johnson, J. A. (2025). Magnetic Nanoparticles and Drug Delivery Systems for Anti-Cancer Applications: A Review. Nanomaterials, 15(4), 285.

Hajiakbari, M., Mahdavi Nejad, A., & Houshfar, E. (2024). Enhancing diesel engine cooling efficiency: A comprehensive numerical study on nanofluid coolants with exergy and economic analysis. Case Studies in Thermal Engineering, 56, 104217.

Hamzat, A. K., Omisanya, M. I., Sahin, A. Z., Ropo Oyetunji, O., & Abolade Olaitan,

N. (2022). Application of nanofluid in solar energy harvesting devices: A comprehensive review. Energy Conversion and Management, 266, 115790.

Hou, Y., Sun, Z., Rao, W., & Liu, J. (2018). Nanoparticle-mediated cryosurgery for tumor therapy. Nanomedicine: Nanotechnology, Biology and Medicine, 14(2), 493–506.

Jang, S. P., & Choi, S. U. S. (2006). Cooling performance of a microchannel heat sink with nanofluids. Applied Thermal Engineering, 26(17), 2457–2463.

Jin, C., Wang, K., Oppong-Gyebi, A., & Hu, J. (2020). Application of Nanotechnology in Cancer Diagnosis and Therapy—A Mini-Review. International Journal of Medical Sciences, 17(18), 2964–2973.

Kao, M. J., Lo, C. H., Tsung, T. T., Wu, Y. Y., Jwo, C. S., & Lin, H. M. (2007).

Copper-oxide brake nanofluid manufactured using arc-submerged nanoparticle synthesis system. Journal of Alloys and Compounds, 434–435, 672–674.

Kao, M.-J., Chang, H., Wu, Y.-Y., Tsung, T.-T., & Lin, H.-M. (2007). Producing Aluminum-oxide brake nanofluids using plasma charging system. Journal of the Chinese Society of Mechanical Engineers, 28(2), 123–131.

Khashaei, A., Ameri, M., & Azizifar, S. (2024). Heat transfer enhancement and pressure drop performance of Al2O3 nanofluid in a laminar flow tube with deep dimples under constant heat flux: An experimental approach. International Journal of Thermofluids, 24, 100827.

Kim, E.-H., Park, S., & Bae, O.-N. (2025). Cardiovascular Toxicity of Metal-Based Nanoparticles. International Journal of Molecular Sciences, 26(12), 5816.

Lekamge, S., Ball, A. S., Shukla, R., & Nugegoda, D. (2020). The Toxicity of Nanoparticles to Organisms in Freshwater. In P. de Voogt (Ed.), Reviews of Environmental Contamination and Toxicology Volume 248 (pp. 1–80). Springer International Publishing.

López-Barrera, E. A., Grotzner, S. R., Esquivel, L., Voigt, C. L., Campos, S. X., & Ribeiro, C. A. de O. (2021). Histopathological effects of silver nanoparticles in Rhamdia quelen after oral exposure. Ecotoxicology and Environmental Contamination, 16(1), 83–89.

Loza, K., Epple, M., & Maskos, M. (2019). Stability of Nanoparticle Dispersions and Particle Agglomeration. In P. Gehr & R. Zellner (Eds.), Biological Responses to Nanoscale Particles: Molecular and Cellular Aspects and Methodological Approaches (pp. 85–100). Springer International Publishing.

Ma, J., Lu, G., Huang, X., & Feng, C. (2021). π-Conjugated-polymer-based nanofibers through living crystallization-driven self-assembly: Preparation, properties and applications. Chemical Communications, 57(98), 13259–13274.

McCallen, R. C., Salari, K., Ortega, J., Castellucci, P., Pointer, W. D., Chang, J., Singh, S., Dringenberg, E., Browand, F., Radovich, C., Merzel, T., Plocher, D., Ross, J., & Storms, B. (2007). DOE Project on Heavy Vehicle Aerodynamic Drag (No. UCRL--TR-227076). Lawrence Livermore National Laboratory (LLNL), Livermore, CA (United States); Argonne National Laboratory (ANL), Argonne, IL (United States); NASA Ames Research Center (ARC), Moffett Field, Mountain View, CA (United States).

Meng, B., Yan, G., He, P., Zhou, Q., Xu, W., & Qiao, Y. (2025). Nanotechnology applications in geothermal energy systems: Advances, challenges and opportunities. Advances in Geo-Energy Research, 15(2), 172–180.

Murshed, S. M. S. (2025). Thermal Properties and Features of Nanofluids.

Nanomaterials, 15(5), 334.

Namburu, P. K., Das, D. K., Tanguturi, K. M., & Vajjha, R. S. (2009). Numerical study of turbulent flow and heat transfer characteristics of nanofluids considering variable properties. International Journal of Thermal Sciences, 48(2), 290–302.

Nanan Kwanchai, Chuwattanakul Varesa, Pramuanjaroenkij Anchasa, & Eiamsa-Ard Smith. (2024). Effect of a TiO2/water Nanofluid on the Thermal Cooling of a Central Processing Unit. Chemical Engineering Transactions, 109, 595–600.

Nguyen, L. V., Kosinski, P., Balakin, B. V., & Kosinska, A. (2023). Direct absorption solar collector: Use of nanofluids and biodegradable colloids. International Journal of Thermal Sciences, 190, 108292.

Okello, J. A., Mutuku, W. N., & Oyem, A. O. (2020). A Review of Nanofluids Synthesis, Factors Influencing Their Thermophysical Properties and Applications. Journal of Engineering Research and Reports.

Okello, J. A., Oyem, A. O., & Mutuku, W. N. (2021). Examination of Engine oil-based ((MWCNTs-TiO2), (MWCNTs- Al2O3), (MWCNTs-Cu)) Hybrid Nanofluids for Optimal Nanolubricant. IOSR Journal of Mathematics, 17(2), 24–38.

Popa, I., Gillies, G., Papastavrou, G., & Borkovec, M. (2010). Attractive and Repulsive Electrostatic Forces between Positively Charged Latex Particles in the Presence of Anionic Linear Polyelectrolytes. The Journal of Physical Chemistry B, 114(9), 3170–3177.

Rahman, M. A., Hasnain, S. M. M., Pandey, S., Tapalova, A., Akylbekov, N., & Zairov, R. (2024). Review on Nanofluids: Preparation, Properties, Stability, and Thermal Performance Augmentation in Heat Transfer Applications. ACS Omega, 9(30), 32328–32349.

Ramadhan, A. I., Azmi, W. H., & Mamat, R. (2020). Heat transfer characteristics of car radiator using tri-hybrid nanocoolant. IOP Conference Series: Materials Science and Engineering, 863(1), 012054.

Rarokar, N., Yadav, S., Saoji, S., Bramhe, P., Agade, R., Gurav, S., Khedekar, P., Subramaniyan, V., Wong, L. S., & Kumarasamy, V. (2024). Magnetic nanosystem a tool for targeted delivery and diagnostic application: Current challenges and recent advancement. International Journal of Pharmaceutics: X, 7, 100231.

Razzaq, I., Xinhua, W., Rasool, G., Sun, T., Shflot, A. S., Malik, M. Y., Abbas, K., Ali, S., & Ali, A. (2025). Nanofluids for Advanced Applications: A Comprehensive Review on Preparation Methods, Properties, and Environmental Impact. ACS Omega, 10(6), 5251–5282.

Rezvani, A., Kichigin, A., Zubiri, B. A., Spiecker, E., & Segets, D. (2025). Insights into Stability and Selective Agglomeration in Binary Mixtures of Colloids: A

Study on Gold Nanoparticles and Ultra-Small Quantum Dots. Powders, 4(1), 9.

Riaz, S., Ali, S., Summer, M., Akhtar, U., Noor, S., Haqqi, R., Farooq, M. A., & Sardar, I. (2025). Multifunctional Magnetic Nanoparticles for Targeted Drug Delivery Against Cancer: A Review of Mechanisms, Applications, Consequences, Limitations, and Tailoring Strategies. Annals of Biomedical Engineering, 53(6), 1291–1327.

Rohaizan, M. A. M., Sidik, N. A. C., & M’hamed, B. (2023). Thermal Properties Investigation of Nanocellulose for Liquid Cooling. Journal of Advanced Research Design, 108(1), 1–11.

Sani, E., Barison, S., Pagura, C., Mercatelli, L., Sansoni, P., Fontani, D., Jafrancesco, D., & Francini, F. (2010). Carbon nanohorns-based nanofluids as direct sunlight absorbers. Optics Express, 18(5), 5179–5187.

Sharma, T., Mohana Reddy, A. L., Chandra, T. S., & Ramaprabhu, S. (2008). Development of carbon nanotubes and nanofluids based microbial fuel cell. International Journal of Hydrogen Energy, 33(22), 6749–6754.

Shiravi, A. H., Firoozzadeh, M., Bostani, H., Shafiee, M., & Bozorgmehrian, M. (2020). Experimental study on carbon nanofluid pressure drop and pumping power. Advances in Nanochemistry, 2(1), 27–31.

Subhedar, D. G., Ramani, B. M., Chauhan, K. V., Panchal, H., Prajapati, S. M., Al- rubaie, A. J., & Jaber, M. M. (2024). Experimental study on the variation of car radiator frontal area using Al2O3/water-ethylene glycol nano coolant. Proceedings of the Institution of Mechanical Engineers, Part E: Journal of Process Mechanical Engineering, 238(4), 1800–1808.

Sultana, A., Zare, M., Thomas, V., Kumar, T. S. S., & Ramakrishna, S. (2022). Nano- based drug delivery systems: Conventional drug delivery routes, recent developments and future prospects. Medicine in Drug Discovery, 15, 100134.

Sun, W., Wang, C., Tian, C., Li, X., Hu, X., & Liu, S. (2023). Nanotechnology for brain tumor imaging and therapy based on π-conjugated materials: State-of- the-art advances and prospects. Frontiers in Chemistry, 11.

Ungar, E., & Erickson, L. (2011). Assessment of the Use of Nanofluids in Spacecraft Active Thermal Control Systems. In AIAA SPACE 2011 Conference & Exposition. American Institute of Aeronautics and Astronautics.

Wang, B., Hu, S., Teng, Y., Chen, J., Wang, H., Xu, Y., Wang, K., Xu, J., Cheng, Y., & Gao, X. (2024). Current advance of nanotechnology in diagnosis and treatment for malignant tumors. Signal Transduction and Targeted Therapy, 9(1), 200.

Wang, D., Ali, M. A., Sharma, K., Almojil, S. F., Alizadeh, A., Alali, A. F., & Almohana, A. I. (2023). Multiphase numerical simulation of exergy loss and thermo-hydraulic behavior with environmental cosiderations of a hybrid nanofluid in a shell-and-tube heat exchanger with twisted tape. Engineering Analysis with Boundary Elements, 147, 1–10.

Yousef, M. I., Abuzreda, A. A., & Kamel, M. A.-N. (2019). Cardiotoxicity and lung toxicity in male rats induced by long-term exposure to iron oxide and silver nanoparticles. Experimental and Therapeutic Medicine, 18(6), 4329–4339.

Yousef, M. I., Roychoudhury, S., Jafaar, K. S., Slama, P., Kesari, K. K., & Kamel, M. A.-N. (2022). Aluminum oxide and zinc oxide induced nanotoxicity in rat brain, heart, and lung. Physiological Research, 71(5), 677–694.

Zahra Haeri, S., Khiadani, M., Ramezanzadeh, B., Kariman, H., & Zargar, M. (2025). Photo-thermal conversion properties of hybrid NH2-MIL-125/TiN/EG nanofluids for solar energy harvesting. Applied Thermal Engineering, 258, 124607.

Zhou, J., Wu, Z., Zhang, Z., Liu, W., & Xue, Q. (2000). Tribological behavior and lubricating mechanism of Cu nanoparticles in oil. Tribology Letters, 8(4), 213– 218.