Review Article

BIOINSPIRED POLYMER METAL COMPLEX COMPOSITES: FABRICATION, MULTIFUNCTIONALITY, AND EMERGING APPLICATIONS

ABSTRACT

Polymer–metal complex composites have emerged as a dynamic class of hybrid materials that merge the structural versatility of polymers with the functional tunability of metal coordination compounds. This review provides a comprehensive overview of recent developments in the design, synthesis, and application of such composites, with a special emphasis on the use of natural and bio-based ligands. Various preparation techniques including solution casting, in situ complexation, melt blending, electrospinning, and sol gel methods are discussed, highlighting their influence on composite morphology and performance. The integration of metal complexes into polymer matrices has been shown to significantly enhance mechanical, thermal, barrier, catalytic, and biological properties, enabling advanced applications in fields such as biomedicine, packaging, catalysis, and environmental remediation. However, several challenges persist, including poor dispersion, interfacial incompatibility, thermal instability of ligands, and metal ion leaching. Emerging strategies such as surface functionalization, reactive processing, and the incorporation of metal–organic frameworks (MOFs) and smart ligands are actively addressing these limitations. The review also compares natural versus synthetic ligands, evaluating their coordination behavior, environmental compatibility, and functional outcomes. Recent innovations in stimuli-responsive systems, nanostructuring, and green processing are paving the way for next-generation polymer–metal composites with enhanced multifunctionality and sustainability.

Keywords:  Polymer composites, Metal complexes, Natural ligands, Material properties, Green synthesis

INTRODUCTION

Polymer–metal complex composites represent a rapidly growing area in materials science, combining the structural flexibility of polymers with the functional versatility of coordination chemistry. The integration of metal complexes into polymer matrices enables the development of multifunctional materials with enhanced thermal, mechanical, optical, barrier, and biological properties[1]. These composites are widely explored for applications in biomedical devices, catalysis, electronics, active packaging, and environmental remediation. By coordinating metal ions with synthetic or natural ligands like EDTA, tannic acid, or flavonoids, their physicochemical and biofunctional characteristics can be precisely tuned. Despite these advantages, challenges such as poor dispersion, interfacial incompatibility, and metal ion leaching often limit performance and stability. Recent progress in processing methods including electrospinning, reactive extrusion, and surface functionalization has significantly improved the uniform distribution and retention of metal complexes in polymer matrices[2,3]. Additionally, the emergence of nanocomposites incorporating metal–organic frameworks (MOFs), graphene–metal complexes, and bioinspired ligands has opened new directions for high-performance and sustainable systems. This review provides an overview of the current developments, key properties and applications of polymer–metal complex composites, emphasizing their potential in next-generation smart and eco-friendly materials[4].

Ligands

A ligand is a molecule or ion that binds to a metal ion to form a coordination complex. Ligands do this by donating one or more pairs of electrons to the metal, typically through atoms like oxygen, nitrogen, or sulfur[5]. This interaction forms a coordinate (dative) bond, where both electrons in the bond come from the ligand. Synthetic ligands are man-made molecules specifically designed to bind metal ions and form stable coordination complexes. They are engineered in the laboratory with precise molecular structures, denticity (number of donor atoms), and functional groups to achieve desired chemical or physical properties. Synthetic ligands often offer higher stability, predictability, and versatility than natural ligands[6]. Natural ligands used in polymer–metal complex systems are predominantly derived from plant-based polyphenols, flavonoids, alkaloids, and organic acids, which possess abundant electron-donating functional groups such as hydroxyl (–OH), carboxyl (–COOH), and carbonyl (C=O) groups[7]. Common sources include tannins from tree bark and fruits, gallic acid and ellagic acid from berries and tea, curcumin from turmeric, catechins from green tea, and quercetin from onions and apples. These ligands typically exhibit bidentate or multidentate coordination modes, allowing them to chelate metal ions like Fe³⁺, Cu²⁺, Zn²⁺, and Ag⁺ with high stability[8]. Based on their electron-donating ability and coordination behavior, they are classified as neutral ligands (e.g., curcumin), anionic ligands (e.g., gallic acid, tannic acid), or zwitterionic ligands (e.g., amino acids). Their natural origin not only ensures biocompatibility and biodegradability but also introduces intrinsic antioxidant, antimicrobial, and UV-absorbing properties to the resulting metal–polymer complexes, making them suitable for biomedical, food packaging, and catalytic applications. The table: 1 gives the comparison and natural and synthetic ligands[9].

Table:1 Comparison natural and synthetic ligands[10,11]

| Feature | Natural Ligands | Synthetic Ligands |
| --- | --- | --- |
| Origin | Plant, microbial, animal sources | Laboratory-synthesized compounds |
| Examples | Tannic acid, curcumin, gallic acid | EDTA, bipyridine, Schiff bases |
| Coordination | Multi-dentate, via –OH, –COOH, –NH₂ | Customizable mono-/multi-dentate |
| Bioactivity | High (antioxidant, antimicrobial) | Low (unless functionalized) |
| Environmental Impact | Biodegradable, eco-friendly | Non-biodegradable, sometimes toxic |
| Stability | Moderate (may degrade thermally) | High thermal/chemical stability |
| Applications | Biomedical, packaging, green materials | Catalysis, sensing, industrial materials |

Classification of Ligands

Ligands employed in polymer–metal complex composites can be systematically categorized into four major classes natural, synthetic, biopolymeric, and drug-based based on their origin, structural characteristics, and functional relevance to target applications. Figure 1 displays flow chart of types of ligans[12].

- Natural ligands encompass bio-derived molecules such as amino acids, short peptides, polyphenols (e.g., tannic acid, gallic acid), chlorophyll derivatives, and vitamins. These ligands are sourced from plants, microbes, or animal tissues and are favored for their eco-compatibility, intrinsic biocompatibility, and availability of functional groups (–OH, –COOH, –NH₂) that readily participate in metal coordination. They not only stabilize the metal centers but also impart antioxidant or antimicrobial properties. Table 2. provides natural ligands, their metal complexes, coordination properties, and potential applications[13].

- Synthetic ligands include structurally engineered molecules like Schiff bases, phosphines, crown ethers, and porphyrins, which are either chemically synthesized or modified from natural templates[14]. These ligands offer superior control over coordination geometry, electronic distribution, and stability of metal complexes. Their tunable steric and electronic environments enable precise modulation of catalytic activity, redox potential, and metal selectivity, which is essential in electronics, catalysis, and sensor applications[15].

- Biopolymeric ligands consist of high-molecular-weight natural polymers such as chitosan, alginate, pectin, silk fibroin, gelatin, and cellulose derivatives. These macromolecular ligands provide multiple coordination sites along their backbone, supporting chelation with multivalent metal ions. Besides coordinating capability, they contribute significantly to the mechanical integrity, film-forming ability, and biodegradability of the composites[16].

- Drug-based ligands represent a class of bioactive small molecules including quercetin, curcumin, isatin, and ciprofloxacin, which not only coordinate with metal ions but also impart therapeutic functionalities. These ligands are widely applied in biomedical composites due to their pharmacological properties such as antimicrobial, anticancer, or anti-inflammatory effects coupled with the controlled metal ion release behavior that enhances their efficacy in localized therapy or bioactive coatings[17].

Figure:1 Flow chart of types of ligands

Table: 2 Summary of natural compound or extract–metal ion complexes, showing their metal charge states, coordination behaviors, resulting physicochemical properties, and potential applications [ 18-48]

| Natural Compound / Extract | Chemical Formula | Metal Ion (Charge) | Coordination Behavior | Denticity | Properties | Applications |
| --- | --- | --- | --- | --- | --- | --- |
| Curcumin (Turmeric) | C₂₁H₂₀O₆ | Cu(II), Zn(II), Fe(III), Ni(II) | Electron donor via β-diketone & phenolic –OH | Bidentate | Enhanced stability, bioavailability, DNA binding | Anticancer, antioxidant, antimicrobial |
| Quercetin (Onion, tea, peels) | C₁₅H₁₀O₇ | Cu(II), Zn(II), Co(II), Fe(III) | Polyphenolic donor, strong chelator | Bidentate to tridentate | High ROS scavenging, metal ion chelation | Antioxidant, anti-inflammatory, enzyme inhibition |
| Catechin (Green tea) | C₁₅H₁₄O₆ | Fe(III), Cu(II) | Electron donor via hydroxyl groups | Bidentate | Redox-active complexes, radical scavenging | Antioxidant, neuroprotective |
| Chlorogenic acid (Coffee, berries) | C₁₆H₁₈O₉ | Co(II), Mg(II), Mn(II), Ni(II), Sr(II) | Donor via carboxyl and phenol | Tridentate | Enzyme inhibition, α-amylase/α-glucosidase | Antidiabetic, antibacterial |
| Gallic acid (Gallnuts, tea) | C₇H₆O₅ | Ca(II), Cu(II), Zn(III), Cr(III), Se(IV) | Donor via 3 phenolic –OH | Tridentate | Chelation, ROS modulation | Antioxidant, wound healing, anticancer |
| Aloe vera extract | C₁₀H₁₆O₁₀ₙ (polysaccharides) | Cu(II), Zn(II), Fe(II) | Donor from sugars, carboxyls | Variable (mono–tridentate) | Green reducing/capping agent | Antibacterial, wound healing, larvicidal |
| Flavonoids (mixed) | C₁₅H₁₂O₆ (general) | Mn(II), Zn(II), Co(II), Ni(II) | π–donor ligands with OH and C=O | Bidentate to tetradentate | Metal-ligand charge transfer | Antiviral, anticancer, enzyme inhibition |
| Tannic acid (Oak bark, tea) | C₇₆H₅₂O₄₆ | Fe(II), Co(II) | Polyphenolic donor, strong chelator | Polydentate | Crosslinking, precipitation, protein binding | Antimicrobial, water purification |
| Lignin derivatives | C₉H₁₀O₂ (phenylpropanoid unit) | Fe(III), Cu(II) | Aromatic alcohol donor | Polydentate | Biodegradable, electron transfer | Adsorption, catalysis, antimicrobial |
| Caffeic acid (Coffee, fruits) | C₉H₈O₄ | Cu(II), Pb, Mg | Phenolic/π-conjugated donor | Bidentate | Radical neutralization | Antioxidant, cytotoxicity |
| Berberine (Berberis) | C₂₀H₁₈NO₄⁺ | Zn(II), Cu(II) | Nitrogen-containing donor | Bidentate | Intercalates DNA, enhances bioactivity | Antibacterial, anticancer |
| Rutin (Citrus peel) | C₂₇H₃₀O₁₆ | Zn(II), Cu(II), Ni(II), Zr(II) | Polyphenolic –OH donor | Bidentate | Improved pharmacological action | Antidiabetic, antioxidant |
| Eugenol (Clove oil) | C₁₀H₁₂O₂ | Co(II), Fe(II), Ni(II) | Electron-rich phenol and ether | Monodentate to bidentate | Lipophilic complexes, bioactive | Antifungal, analgesic |
| Emodin (Aloe, rhubarb) | C₁₅H₁₀O₅ | Cu(II), Fe(II), Mn(II) | π-conjugated + phenolic OH | Bidentate | DNA damage, antiproliferative | Anticancer, anti-inflammatory |
| Asiatic acid (Centella asiatica) | C₃₀H₄₈O₅ | Cu(II), Zn(II) | Carboxyl donor, steroid-like | Bidentate | Bio-scaffold, wound healing | Anti-aging, skin regeneration |
| Thymol (Thyme oil) | C₁₀H₁₄O | Cu(II), Zn(II) | Phenolic donor | Monodentate | ROS induction, permeability | Antibacterial, antifungal |
| Apigenin (Chamomile, parsley) | C₁₅H₁₀O₅ | Fe(III), Cu(II) | OH/C=O donor | Bidentate | Enhanced cytotoxicity | Anticancer, neuroprotective |
| Resveratrol (Red wine, grapes) | C₁₄H₁₂O₃ | Cu(I) | Phenolic donor, π-system | Bidentate | DNA protection, ROS scavenging | Antioxidant, anticancer |
| Piperine (Black pepper) | C₁₇H₁₉NO₃ | Zn(II) | π-electron rich alkaloid | Bidentate | Drug bioenhancer | Antimicrobial, solubility enhancer |
| Betulinic acid (Birch bark) | C₃₀H₄₈O₃ | Cu(II), Zn(II) | Carboxyl donor, pentacyclic structure | Bidentate | Induces apoptosis | Antiviral, anticancer |
| Silymarin (Milk thistle) | C₂₅H₂₂O₁₀ (silybin) | Cu(II), Zn(II), Fe(III) | Polyphenol + flavonol donors | Bidentate | ROS neutralization | Hepatoprotective, antioxidant |
| Isatin (Indole alkaloid) | C₈H₅NO₂ | Cu(II), Ni(II), Co(II) | C=O and N donor | Bidentate | Enzyme inhibition, DNA intercalation | Antiviral, anticancer |
| Hesperidin (Citrus fruits) | C₂₈H₃₄O₁₅ | Cu(II), Zn(II) | Polyhydroxyl donor | Bidentate | Redox modulation | Antidiabetic, antioxidant |
| Cinnamic acid (Cinnamon) | C₉H₈O₂ | Zn(II), Cd(II), Hg(I) | Carboxylate and π-electron donor | Monodentate to bidentate | Complex stability, redox activity | Antioxidant, antibacterial |
| Kaempferol (Broccoli, tea) | C₁₅H₁₀O₆ | Ru(II) | OH and C=O donor | Bidentate | Chelation via phenol groups | Antioxidant, anticancer |
| Gingerol (Ginger) | C₁₇H₂₆O₄ | Ag(II), Au(II), Cu(II) | Phenolic OH, ketone donor | Bidentate | Bioavailability, wound repair | Anticancer |
| Myricetin (Berries, tea) | C₁₅H₁₀O₈ | Zn(II), Fe(III) | Multiple OH donors | Tridentate | Improves ROS scavenging | Antioxidant, anticancer |
| Vanillin (Vanilla bean) | C₈H₈O₃ | Cu(II), Zn(II), Fe(II) | Aldehyde/Schiff base formation | Bidentate (via Schiff base) | Schiff base-metal complexation | Antioxidant, antimicrobial |
| Alizarin (Madder root) | C₁₄H₈O₄ | Cu(II), Zn(II), Fe(III) | Anthraquinone + OH donor | Bidentate | DNA intercalation, π-stacking | Textile dye, antifungal, anticancer |
| Luteolin (Celery, thyme) | C₁₅H₁₀O₆ | Fe(III), Al(III), Cu(II) | Polyhydroxy flavone | Bidentate | Enhances brain-targeted delivery | Neuroprotective, antioxidant |
| Baicalein (Scutellaria root) | C₁₅H₁₀O₅ | Cu(II) | Phenolic groups | Bidentate | Mitochondrial disruption | Antioxidant |
| Tea polyphenols (Camellia sinensis) | C₁₅H₁₄O₆ (general) | Ag(I), Au(III), Cu(II) | Reducing agent + OH donors | Polydentate | Reduces/stabilizes metals | Anticancer, green nanoparticle synthesis |

PROCESSING METHODS OF POLYMER–METAL COMPLEX COMPOSITES

Recent years have witnessed significant progress in the development of polymer–metal complex composites, driven by advancements in ligand engineering, nanotechnology, and green processing techniques[49]. Researchers are increasingly utilizing bio-based ligands such as polyphenols (e.g., tannic acid, gallic acid), amino acids, and flavonoids to form stable metal complexes with enhanced biocompatibility and reduced toxicity, aligning with sustainable material goals. Innovations in in situ complexation during processing have improved the dispersion and interfacial bonding of metal complexes within polymer matrices, particularly in systems such as PLA, chitosan, PVA, and PEG. Electrospinning has emerged as a cutting-edge method for producing nanofiber mats with embedded metal complexes for applications in wound healing, catalysis, and filtration[50]. Additionally, metal–organic frameworks (MOFs) and graphene–metal hybrids have been incorporated into polymers to create multifunctional composites with high surface area, controlled porosity, and tunable electrical, thermal, or antimicrobial properties. Recent studies have also reported stimuli-responsive composites that alter their behavior in response to pH, light, or temperature, opening new possibilities for smart biomedical devices and sensors. Furthermore, the application of reactive extrusion, supercritical CO₂-assisted processing, and machine learning-guided material design are advancing the scalability and performance predictability of these composites[51]. Collectively, these innovations are transforming polymer–metal complex systems from academic curiosity to versatile platforms for environmental, biomedical, packaging, and electronic applications.

PROPERTIES OF POLYMER METAL COMPLEX COMPOSITES

Polymer–metal complex composites show a wide range of useful properties. Their biological properties include strong antimicrobial, antioxidant, anti-inflammatory, and anticancer effects. These arise from interactions between metal ions such as Ag⁺, Zn²⁺, Cu²⁺, and Fe³⁺ with natural ligands like tannic acid and quercetin. Such interactions enhance cell compatibility and support wound healing and tissue regeneration. The mechanical properties are improved through metal-ion coordination, which increases tensile strength, stiffness, and structural stability. The incorporation of biocompatible plasticizers such as vegetable oils, glycerol or polyethylene glycol that balance rigid and flexible phases within the composite[52]. The thermal properties are also enhanced due to stable metal–ligand bonds that raise glass transition and decomposition temperatures, improving heat resistance and flame retardancy. Nevertheless, excessive metal loading may result in residual inorganic ash and reduced melt processability. These limitations can be addressed through the incorporation of green compatibilizers or synergistic nano-reinforcements, such as clay, lignin, or biogenic silica, to maintain thermal benefits while ensuring processing efficiency and material homogeneity. These composites have better barrier properties, reducing gas and moisture permeability and providing UV protection.  Complexes such as gallic acid–Fe³⁺ and tannic acid–Cu²⁺ integrated into poly(vinyl alcohol) or polysaccharide-based systems have demonstrated substantial reductions in water vapor transmission rates (WVTR), often exceeding 30–40%, while also imparting UV-shielding and oxidative stability. This type of composites also have excellent catalytic properties, effectively supporting photocatalysis, pollutant degradation, and biosensing[53].

APPLICATIONS OF METAL COMPLEXES IN POLYMER COMPOSITES

Biomedical Applications

Polymer–metal complex composites represent a rapidly advancing class of materials in biomedical engineering, offering multifunctionality for wound healing, tissue regeneration, antimicrobial coatings, and controlled drug delivery. The coordination of bioactive metal ions such as Ag⁺, Cu²⁺, Zn²⁺, Fe³⁺, and Ca²⁺ with biocompatible polymers particularly natural and semi-synthetic matrices like chitosan and poly(vinyl alcohol) in combination with polyphenolic ligands including curcumin and tannic acid, has been shown to impart superior antibacterial, anti-inflammatory, and antioxidant activities[54]. These multifunctional attributes support key physiological processes such as cellular adhesion, migration, proliferation, and hemostasis, thereby enhancing epithelial closure and tissue remodeling. Structurally, these composites enable a tunable release of metal ions, allowing localized therapeutic action while minimizing systemic cytotoxicity. Recent developments in nanoscale engineering have further improved their bioavailability, degradation kinetics, and responsiveness to physiological stimuli such as pH and enzymatic activity. In bone tissue engineering, Fe³⁺- and Ca²⁺-based coordination systems have demonstrated enhanced osteoinductive potential by stimulating alkaline phosphatase expression, collagen matrix deposition, and mineralized nodule formation. Collectively, these advances establish polymer–metal complexes as highly promising candidates for next-generation regenerative therapies and implantable biomedical devices[55].

Food Packaging and Preservation

Polymer–metal complex systems have garnered significant attention in food packaging applications due to their synergistic barrier, antimicrobial, and antioxidant functionalities. The coordination of metal ions with bioactive ligands, particularly natural polyphenols, results in matrices capable of reducing oxygen and moisture permeability, thereby retarding lipid oxidation and microbial proliferation. These active packaging systems create an inhospitable environment for spoilage organisms by facilitating the gradual and localized release of metal ions, which disrupt microbial cell membranes and interfere with enzymatic activity. Incorporation of such complexes into biodegradable polymer films, such as polylactic acid, poly(vinyl alcohol), enhances their physicochemical stability while maintaining transparency and flexibility essential for food contact applications[56]. Moreover, the integration of pH-sensitive metal–ligand interactions into packaging films enables the development of intelligent packaging systems that visually indicate spoilage through distinct colorimetric shifts. This dual-functionality not only prolongs shelf life but also enhances consumer safety and product traceability. As a result, polymer–metal complexes represent a promising strategy for the next generation of sustainable, smart food packaging technologies.

Environmental Remediation

Polymer–metal complex composites exhibit considerable potential in environmental remediation, particularly in advanced wastewater treatment and the catalytic degradation of organic contaminants. The integration of redox-active metal ions such as Fe³⁺, Cu²⁺, and Mn²⁺ within polymeric matrices coordinated with phenolic ligands such as catechin, gallic acid, or tannic acid confers intrinsic catalytic activity analogous to natural peroxidases or Fenton-type systems[57]. These coordination complexes enable the activation of hydrogen peroxide or persulfate to generate reactive oxygen species (ROS), such as hydroxyl or sulfate radicals, which drive the efficient oxidative decomposition of persistent contaminants including azo dyes, endocrine disruptors, and pharmaceutical residues[58]. The polymeric immobilization of metal complexes not only enhances catalytic efficiency but also significantly reduces metal ion leaching, and promoting controlled electron transfer. This structural confinement also improves accessibility to active sites, resulting in higher turnover frequency and operational robustness under variable pH and pollutant concentrations. Furthermore, the electron-donating functionality of natural ligands contributes to sustainable redox cycling and enhances complexation stability, enabling prolonged catalytic lifespans. These polymer–metal hybrids thus function as heterogeneous, recyclable catalysts with high substrate selectivity and minimal secondary pollution[59].

Electronics and Sensors

Polymer–metal complex systems are increasingly being explored for applications in flexible electronics, electrochemical sensors, and energy storage devices, owing to their intrinsic redox activity, tunable conductivity, and functional surface chemistry. The incorporation of transition metal ions such as Fe³⁺ or Cu²⁺ into polymer matrices, coordinated through natural polyphenolic ligands, facilitates efficient charge transfer and electron mobility, critical for signal transduction in sensing applications. These materials can be engineered into flexible and stretchable films that respond to environmental stimuli such as humidity, glucose concentration, or volatile organic compounds, with the redox-active metal centers serving as the transducing elements[60]. Natural ligands enhance metal dispersion and interfacial compatibility, contributing to improved electrochemical stability and reproducibility. Moreover, coordination-induced doping has been shown to modulate the dielectric, thermal, and conductivity profiles of the polymer matrix, enabling their integration into energy storage systems such as capacitors and supercapacitors. These modifications also enhance the structural integrity and cycling performance under operational stress. The structural versatility and multifunctionality of polymer–metal complexes thus make them ideal candidates for next-generation wearable sensors, bioelectronic interfaces, and smart energy devices[61].

Catalysis and Smart Coatings

Polymer–metal complex composites are increasingly utilized in multifunctional coating technologies, offering integrated anticorrosive, antimicrobial, catalytic, and self-responsive properties. Coordination networks formed between metal ions such as Fe³⁺ and bio-derived ligands like tannic acid impart durable adhesion, UV shielding, and self-healing characteristics, while simultaneously inhibiting oxidative degradation and corrosion. These coatings are particularly effective in metal surface protection, biomedical implants, and packaging applications where environmental resilience is essential[62]. In catalytic systems, the redox-active nature of the metal centers enables enzyme-mimetic activity, supporting selective oxidation, reduction, or hydrolysis reactions relevant to biosensing and green synthetic chemistry. Smart coatings that use dynamic metal–ligand coordination can respond to environmental changes, such as pH, temperature, or redox conditions. These triggers enable controlled release of active substances (cargo), adaptive surface wettability, and antimicrobial activation[63].

Conclusion

Polymer–metal complex composites represent a promising class of hybrid materials that synergistically combine the processability and flexibility of polymers with the unique functionalities of metal complexes, such as catalytic activity, antimicrobial behavior, electrical conductivity, and structural reinforcement. Recent advances have demonstrated the potential of both natural and synthetic ligands to coordinate metal ions and impart tailored properties to biocompatible or high-performance polymer matrices. However, challenges related to thermal stability, dispersion, interfacial compatibility, leaching, and scalability still limit their widespread application. Overcoming these obstacles through advanced ligand engineering, surface modification, and green processing techniques can significantly enhance composite performance and durability.

DISCLAIMER (ARTIFICIAL INTELLIGENCE)

I hereby declare that no generative AI technologies have been used in the writing, editing, or preparation of this manuscript. All content, text, and figures are original and created solely by the authors.

COMPETING INTERESTS

The authors declare that no competing interests exist in relation to this manuscript.

REFERENCE

- Kumar, S., Mohan, B., Musikavanhu, B., Wang, X., Muhammad, R., Yang, X., & Ren, P., 2025. Metal-polymer-coordinated complexes: An expedient class of hybrid functional materials. Coordination Chemistry Reviews, 524, 216286. https://doi.org/10.1016/j.ccr.2024.216286

- Abtahi, S., Hendeniya, N., Mahmud, S. T., Mogbojuri, G., Iheme, C. L., & Chang, B. (2025). Metal-coordinated polymer–inorganic hybrids: Synthesis, properties, and application. Polymers, 17(2), 136. https://doi.org/10.3390/polym17020136

- Bartczak, P., Szylińczuk, K., Tomaszczak, M., & Borysiak, S. (2024). Sustainable and multifunctional polyurethane green composites with renewable materials. Journal of Materials Science, 59, 13541–13557. https://doi.org/10.1007/s10853-024-09992-9

- Tsuchida, E., & Nishide, H. (2007). Polymer-metal complexes and their catalytic activity. In Molecular Properties (Vol. 24, pp. 1–87). Advances in Polymer Science. https://doi.org/10.1007/3-540-08124-0_1

- Yang, Y., Zhang, C., Zhang, C., Shi, Y., Li, J., Johannessen, B., Liang, Y., Zhang, S., Song, Q., Zhang, H., Huang, J., Ke, J., Zhang, L., Song, Q., Zeng, J., Zhang, Y., Geng, Z., Wang, P.-S., Wang, Z., Zeng, J., & Li, F. (2024). Ligand-tuning copper in coordination polymers for efficient electrochemical C–C coupling. Nature Communications, 15, Article 6316. https://doi.org/10.1038/s41467-024-42679-5

- Ogunbiyi, E. O., Kupa, E., Adanma, U. M., & Solomon, N. O. (2024). Comprehensive review of metal complexes and nanocomposites: Synthesis, characterization, and multifaceted biological applications. Engineering Science & Technology Journal, 5(6), 1935–1951. https://doi.org/10.51594/estj/v5i6.1215

- Marx, F., Beccard, M., Ianiro, A., Dodero, A., Neumann, L. N., Stoclet, G., Weder, C., & Schrettl, S. (2023). Structure and properties of metallosupramolecular polymers with a nitrogen-based bidentate ligand. Macromolecules, 56(18), 7320–7331. https://doi.org/10.1021/acs.macromol.3c00503

- El Hankari, S., Bousmina, M., & El Kadib, A. (2019). Biopolymer@metal-organic framework hybrid materials: A critical survey. Progress in Materials Science, 106, 100579. https://doi.org/10.1016/j.pmatsci.2019.100579

- Nikolić, G. S., Ćakić, M., Mitić, Z., & Ilić, L. (2008). Deconvoluted Fourier-transform LN T-IR study of coordination copper(II) compounds with dextran derivatives. Russian Journal of Coordination Chemistry, 34(5), 322–328.

- Leite, D. C., Peres, G., & Silveira, N. (2016). Biopolymer-metal complexes: Recent advances and applications. In A. Méndez-Vilas (Ed.), Polymer science: Research advances, practical applications and educational aspects (pp. 601–610). Badajoz, Spain: Formatex Research Center.

- Abtahi, S., Hendeniya, N., Mahmud, S. T., Mogbojuri, G., Iheme, C. L., & Chang, B. (2025). Metal-coordinated polymer–inorganic hybrids: Synthesis, properties, and application. Polymers, 17(2), 136. https://doi.org/10.3390/polym17020136

- Reddy, M. S. B., Ponnamma, D., Choudhary, R., & Sadasivuni, K. K. (2021). A comparative review of natural and synthetic biopolymer composite scaffolds. Polymers, 13(7), 1105. https://doi.org/10.3390/polym13071105

- Pei, J., Palanisamy, C. P., Natarajan, P. M., Umapathy, V. R., Roy, J. R., Srinivasan, G. P., Panagal, M., & Jayaraman, S. (2024). Curcumin-loaded polymeric nanomaterials as a novel therapeutic strategy for Alzheimer's disease: A comprehensive review. Ageing Research Reviews, 99, 102393. https://doi.org/10.1016/j.arr.2024.102393

- Sharma, Shubham, P. Sudhakara, Jujhar Singh, R. A. Ilyas, M. R. M. Asyraf, and M. R. Razman. 2021. "Critical Review of Biodegradable and Bioactive Polymer Composites for Bone Tissue Engineering and Drug Delivery Applications." Polymers 13 (16): 2623. https://doi.org/10.3390/polym13162623

- Yang, W., Sousa, A. M. M., Thomas-Gahring, A., Fan, X., Jin, T., Li, X., Tomasula, P. M., & Liu, L. (2016). Electrospun polymer nanofibers reinforced by tannic acid/Fe³⁺ complexes. Materials, 9(9), 757. https://doi.org/10.3390/ma9090757

- Nalawade, S. P., Picchioni, F., & Janssen, L. P. B. M. (2006). Supercritical carbon dioxide as a green solvent for processing polymer melts. Progress in Polymer Science, 31(1), 19–43.

- Patsahan, T., & Pizio, O. (2022). Structural aspects of the clustering of curcumin molecules in water: Molecular dynamics computer simulation study. Condensed Matter Physics, 25(2), 23201. https://doi.org/10.5488/CMP.25.23201

- Tsoupras, A., Pafli, S., Stylianoudakis, C., Ladomenou, K., Demopoulos, C. A., & Philippopoulos, A. (2024). Anti-inflammatory and antithrombotic potential of metal-based complexes and porphyrins. Compounds, 4(2), 376–400. https://doi.org/10.3390/compounds4020023

- Stover, K.; Fukuyama, T.; Young, A.T.; Daniele, M.A.; Oberley, R.; Crapo, J.D.; Bäumer, W. Topically Applied Manganese-Porphyrins BMX-001 and BMX-010 Display a Significant Anti-Inflammatory Response in a Mouse Model of Allergic Dermatitis. Arch. Dermatol. Res. 2016, 308, 711–721.

- Abdel-Rahman, L.H.; El-Khatib, R.M.; Abdel-Fatah, S.M.; Moustafa, H.; Alsalme, A.M.; Nafady, A. Novel Cr (III), Fe (III) and Ru (III) Vanillin Based Metallo-Pharmaceuticals for Cancer and Inflammation Treatment: Experimental and Theoretical Studies. Appl. Organomet. Chem. 2019, 33, e5177.

- Rodríguez-Arce, E., & Saldías, M. (2021). Antioxidant properties of flavonoid metal complexes and their potential inclusion in the development of novel strategies for the treatment against neurodegenerative diseases. Biomedicine & Pharmacotherapy, 143, 112236. https://doi.org/10.1016/j.biopha.2021.112236

- Lungu, I. I., Cioanca, O., Mircea, C., Tuchilus, C., Stefanache, A., Huzum, R., & Hancianu, M. (2024). Insights into catechin–copper complex structure and biologic activity modulation. Molecules, 29(20), 4969. https://doi.org/10.3390/molecules29204969

- Zheng, K., Liu, Y., Peng, L., Li, Z., & Xu, W. (2023). Structural characterization of chlorogenic acid-metal complexes derived from the aqueous extracts of medicinal plants and their DNA cleavage and antibacterial activities. Arabian Journal of Chemistry, 16(7), 104835. https://doi.org/10.1016/j.arabjc.2023.104835

- El-Megharbel, S. M., & Hamza, R. Z. (2022). Synthesis, spectroscopic characterizations, conductometric titration and investigation of potent antioxidant activities of gallic acid complexes with Ca(II), Cu(II), Zn(III), Cr(III) and Se(IV) metal ions. Journal of Molecular Liquids, 358, 119196. https://doi.org/10.1016/j.molliq.2022.119196

- Edo, G. I. (2024). Coordination of bioactive phytochemicals from Aloe vera extracts to metal ions; investigation of the metal complexes and bioactive compound formed. BioMetals, 37, 1379–1391. https://doi.org/10.1007/s10534-024-00593-0

- Kasprzak, M. M., Erxleben, A., & Ochocki, J. (2015). Properties and applications of flavonoid metal complexes. RSC Advances, 5(57), 45853–45877. https://doi.org/10.1039/C4RA13547C

- Kasprzak, M. M., Erxleben, A., & Ochocki, J. (2015). Properties and applications of flavonoid metal complexes. RSC Advances, 5(57), 45853–45877. https://doi.org/10.1039/C5RA05069C

- Wang, Y., Chen, S., Zhao, S., Chen, Q., & Zhang, J. (2020). Interfacial coordination assembly of tannic acid with metal ions on three-dimensional nickel hydroxide nanowalls for efficient water splitting. Journal of Materials Chemistry A, 8(31), 15845–15852. https://doi.org/10.1039/D0TA02229B

- Garcia-Valls, R., & Hatton, T. A. (2003). Metal ion complexation with lignin derivatives. Chemical Engineering Journal, 94(2), 99–105. https://doi.org/10.1016/S1385-8947(03)00007-X

- Baidoo, I., Sarbadhikary, P., Abrahamse, H., & George, B. P. (2025). Metal-based nanoplatforms for enhancing the biomedical applications of berberine: Current progress and future directions. Nanomedicine (London), 20(8), 851–868. https://doi.org/10.1080/17435889.2025.2480051

- Prakash, O., Belal, B., Dhanik, J., Verma, A., Joshi, H. C., & Vivekanand. (2020). Biological activities of metal complexes with rutin and bio-conjugate of citrus extract. Universal Journal of Chemistry, 7(1), 1–24. https://doi.org/10.13189/ujc.2020.070101

- Azez, A., Natheer, R., Mohammed, E., & Saleh, M. Y. (2021). Preparation of new complexes of Fe(II), Co(II), Ni(II) and Cu(II) with mixed ligands of ciprofloxacin or levofloxacin with eugenol and study of their chemical and physical properties. Egyptian Journal of Chemistry, 64, Article ID: 63144. https://doi.org/10.21608/ejchem.2021.63144.3352

- Liu, M.-Y., Pan, X.-L., Li, X.-B., & Wu, B. (2021). [Study on the antioxidant activity of aloe-emodin metal complex] [Article in Chinese]. Sichuan Da Xue Xue Bao Yi Xue Ban, 52(2), 241–247. https://doi.org/10.12182/20201160110

- Rasouli, Z., Irani, M., Jafari, S., & Ghavami, R. (2021). Study of interaction of metal ions with methylthymol blue by chemometrics and quantum chemical calculations. Scientific Reports, 11, 6465. https://doi.org/10.1038/s41598-021-85940-w

- Spiegel, M., & Sroka, Z. (2023). Quantum-mechanical characteristics of apigenin: Antiradical, metal chelation and inhibitory properties in physiologically relevant media. Fitoterapia, 164, 105352. https://doi.org/10.1016/j.fitote.2022.105352

- Chiavarino, B., Crestoni, M. E., Fornarini, S., Taioli, S., Mancini, I., & Tosi, P. (2012). Infrared spectroscopy of copper-resveratrol complexes: A joint experimental and theoretical study. The Journal of Chemical Physics, 137(2), 024307. https://doi.org/10.1063/1.4732583

- Parvin, K., Bhattacharya, A., Rasool, M. A., & Pounikar, Y. (2024). Isolation and characterization of piperine from black pepper, zinc-piperine metal complex. International Journal of Research and Analytical Reviews (IJRAR), 11(1), 799. https://www.ijrar.org/viewfull.php?&p_id=IJRAR24A1244

- Batool, A., Muddassir, M., & Shahid, K. (2024). Synthesis of hydrazide derivative of betulinic acid, its organometallic complexes, characterization and bioassay. Chemistry & Biodiversity. Advance online publication. https://doi.org/10.1002/cbdv.202301275

- Paltinean, G.-A., Tomoaia, G., Riga, S., Mocanu, A., & Tomoaia-Cotisel, M. (2022). Silymarin based complexes – A mini review. Academy of Romanian Scientists Annals – Series on Biological Sciences, 11(1), 146–166.

- Hossain, M. S., Khushy, K. A., Latif, M. A., Hossen, Md. F., Asraf, Md. A., Kudrat-E-Zahan, Md., & Abdou, A. (2022). Co(II), Ni(II), and Cu(II) complexes containing isatin-based Schiff base ligand: Synthesis, physicochemical characterization, DFT calculations, antibacterial activity, and molecular docking analysis. Russian Journal of General Chemistry, 92, 2723–2733. https://doi.org/10.1134/S1070363222120222

- Daoud, S., Afifi, F. U., Al-Bakri, A. G., Kasabri, V., & Hamdan, I. I. (2014). Preparation, physicochemical characterization and biological evaluation of some hesperidin metal complexes. Iranian Journal of Pharmaceutical Research, 13(3), 909–918. https://www.ncbi.nlm.nih.gov/pmc/articles/PMC4177651/

- Kalinowska, M., Świsłocka, R., & Lewandowski, W. (2011). Zn(II), Cd(II) and Hg(I) complexes of cinnamic acid: FT-IR, FT-Raman, ¹H and ¹³C NMR studies. Journal of Molecular Structure, 993(1–3), 404–409. https://doi.org/10.1016/j.molstruc.2011.01.063

- Thangavel, P., Viswanath, B., & Kim, S. (2018). Synthesis and characterization of kaempferol-based ruthenium (II) complex: A facile approach for superior anticancer application. Materials Science and Engineering: C, 90, 479–489. https://doi.org/10.1016/j.msec.2018.03.020

- Sungur, Ş., & Uzar, A. (2008). Investigation of complexes tannic acid and myricetin with Fe(III). Spectrochimica Acta Part A: Molecular and Biomolecular Spectroscopy, 69(1), 225–229. https://doi.org/10.1016/j.saa.2007.03.038

- Sharma, V., Ali, S.W. Nanoarchitectonics of Vanillin-Metal Complexes as Eco-friendly Multifunctional Agents on Cellulosic Fabric. J Inorg Organomet Polym 33, 1932–1945 (2023). https://doi.org/10.1007/s10904-023-02611-1

- Fain, V.Y., Zaitsev, B.E. & Ryabov, M.A. Metal Complexes with Alizarin and Alizarin Red S: Electronic Absorption Spectra and Structure of Ligands. Russian Journal of Coordination Chemistry 30, 365–370 (2004). https://doi.org/10.1023/B:RUCO.0000026008.98495.51

- Malacaria, L., La Torre, C., Furia, E., Fazio, A., Caroleo, M. C., Cione, E., Gallelli, L., Marino, T., & Plastina, P. (2022). Aluminum(III), iron(III) and copper(II) complexes of luteolin: Stability, antioxidant, and anti-inflammatory properties. Journal of Molecular Liquids, 345, 117895. https://doi.org/10.1016/j.molliq.2021.117895

- Rajkumar, M., Presley, S. I. D., Govindaraj, P., Kirubakaran, D., Farahim, F., Ali, T., Shkir, M., & Latha, S. (2025). Synthesis of chitosan/PVA/copper oxide nanocomposite using Anacardium occidentale extract and evaluating its antioxidant, antibacterial, anti-inflammatory and cytotoxic activities. Scientific Reports, 15, Article 3931. https://doi.org/10.1038/s41598-025-87932-6

- Zhou, R., Huang, J., Zhang, W., Wang, W., Peng, W., Chen, J., Yu, C., Bo, R., Liu, M., & Li, J. (2024). Multifunctional hydrogel based on polyvinyl alcohol/chitosan/metal polyphenols for facilitating acute and infected wound healing. Materials Today Bio, 29, 101315. https://doi.org/10.1016/j.mtbio.2024.101315

- 54.T. Lan, Y. Dong, J. Shi, X. Wang, Z. Xu, Y. Zhang, L. Jiang, W. Zhou, X. Sui, Advancing self-healing soy protein hydrogel with dynamic Schiff base and metal-ligand bonds for diabetic chronic wound recovery, Aggregate n/a (n.d.) e639. 10.1002/agt2.639.

- 66.X. Liang, L. Ding, J. Ma, J. Li, L. Cao, H. Liu, M. Teng, Z. Li, Y. Peng, H. Chen, Y. Zheng, H. Cheng, G. Liu, Enhanced Mechanical Strength and Sustained Drug Release in Carrier-Free Silver-Coordinated Anthraquinone Natural Antibacterial Anti-Inflammatory Hydrogel for Infectious Wound Healing, Advanced Healthcare Materials n/a (n.d.) 2400841. 10.1002/adhm.202400841.

- Levy, L., Gurov, A., & Radian, A. (2020). The effect of gallic acid interactions with iron-coated clay on surface redox reactivity. Water Research, 184, 116190. https://doi.org/10.1016/j.watres.2020.116190

- Fedenko, V. S., Landi, M., & Shemet, S. A. (2022). Metallophenolomics: A novel integrated approach to study complexation of plant phenolics with metal/metalloid ions. International Journal of Molecular Sciences, 23(19), 11370. https://doi.org/10.3390/ijms231911370

- Liu, J., Bao, S., Ling, Q., Fan, X., & Gu, H. (2022). Ultra-fast preparation of multifunctional conductive hydrogels with high mechanical strength, self-healing and self-adhesive properties based on Tara tannin–Fe³⁺ dynamic redox system for strain sensors applications. Polymer, 240, 124513. https://doi.org/10.1016/j.polymer.2021.124513

- Roh, H., Kim, D.-H., Cho, Y., Jo, Y.-M., del Alamo, J. A., Kulik, H. J., Dincă, M., & Gumyusenge, A. (2024, March 13). Robust chemiresistive behavior in conductive polymer/MOF composites. https://doi.org/10.48550/arXiv.2403.08914

- Liu, Y., Zhang, W., Su, X., He, W., Yang, J., Qin, G., Yu, X., & Chen, Q. (2023). Self-healable, mechanically durable and cold-resistant integrated supercapacitor enabled by dual metallic redox-mediated multiple cross-linking gel polymer electrolyte. Energy, 282, 128777. https://doi.org/10.1016/j.energy.2023.128777

- Anum, S., Sher, M., Khan, M., Shah, L. A., & Yoo, H.-M. (2025). Supramolecular polymer hydrogels through rapid polymerization enabled by tannic acid–silver dual catalysis for next-generation flexible and wearable sensors. ACS Applied Electronic Materials, 7(6), Article e4c02349. https://doi.org/10.1021/acsaelm.4c02349

- Xu, H., Huang, W.-P., Ren, K.-F., & Tang, Y.-M. (2021). Spraying layer-by-layer assembly of tannin–Fe³⁺ and polyethyleneimine for antibacterial coating. Colloids and Interface Science Communications, 42, 100422. https://doi.org/10.1016/j.colcom.2021.100422

- Song, Y., Wang, X., Tang, J., & Li, G. L. (2024). Dynamic polymer/metal–organic framework hybrid microcapsules for self-healing anticorrosion coatings. ACS Applied Materials & Interfaces, 16(49), 68478–68486. https://doi.org/10.1021/acsami.4c16670

- Sathishkumar, G., Gopinath, K., Zhang, K., & Kang, E.-T. (2022). Recent progress in tannic acid-driven antimicrobial/antifouling surface coating strategies. Journal of Materials Chemistry B, 10(14), 2490–2508. https://doi.org/10.1039/D1TB02073K

- Mohammed, H. A., Mohammed, P. A., & Aziz, S. B. (2025). Physical characteristics of polymer composites based on PVA doped with Mn²⁺ metal complexes synthesized by green approach: Insights to linear and optoelectronic optical properties. Oxford Open Materials Science, 5(1).  https://doi.org/10.1093/oxfmat/itaf003

- Alkhayer, G. (2021). Alginate metal complexes and their application. IntechOpen. https://doi.org/10.5772/intechopen.98885

- Kumar, S., Mohan, B., Musikavanhu, B., Wang, X., Muhammad, R., Yang, X., & Ren, P. (2025). Metal-polymer-coordinated complexes: An expedient class of hybrid functional materials. Coordination Chemistry Reviews, 524, 216286. https://doi.org/10.1016/j.ccr.2024.216286