Original Research Article

Numerical Analysis of the Combined Effect of BSF Thickness and Doping on the Performance of an a-Si:H(n⁺)/c-Si(n)/a-Si:H(p⁺) Heterojunction Solar Cell

.

# ABSTRACT

This work numerically investigates how the Back Surface Field (BSF) thickness and doping affect the performance of a double-heterojunction a-Si:H(n⁺)/c-Si(n)/a-Si:H(p⁺) solar cell. We couple the two-diode formalism with TCAD SILVACO-ATLAS drift–diffusion simulations (SRH recombination) under AM1.5G (100 mW·cm⁻², 300 K) and evaluate Voc, Jsc, fill factor (FF), and efficiency η. BSF thickness is swept from 2 to 20 nm for several wafer thicknesses. A shallow optimum emerges around 10-13 nm, where field-effect passivation and rear selectivity sufficiently suppress rear-surface recombination without incurring excessive series resistance. Very thin BSF (2–5 nm) under-passivates the rear interface, keeping recombination high. Beyond ≈13-15 nm, added thickness increases contact/transport resistance and parasitic absorption, which rounds the J-V knee, limits FF, and can depress η. BSF doping is varied from 1×1016 to 1×1020 cm⁻³. Over this range, performance improves modestly yet consistently: Voc rises by ~8 mV (≈0.728→0.736 V) via reduced effective saturation current; Jsc gains ~0.08 mA·cm⁻² as rear recombination drops; and FF increases slightly (≈83.05→83.15%) thanks to better carrier selectivity and lower local series resistance at the rear contact. Combining a 10-13 nm BSF with high doping yields simulated η ≈24.05%. Overall, co-optimizing BSF thickness and doping balances passivation quality, selectivity, and transport, improving η without sacrificing Jsc or FF. Practical guidance: target a few-nanometer BSF near 10-13 nm with sufficiently high doping; use FF-Voc diagnostics to disentangle resistive vs. recombination losses; keep optical stacks identical when benchmarking. Future work will couple opto-thermal modeling with 3D transport including interface traps/bulk defects and extend to thinned wafers to guide ultrathin, high-efficiency SHJ designs.

Keywords: silicon heterojunction (SHJ), Back Surface Field (BSF), field-effect passivation, doping optimization, SILVACO-ATLAS, fill factor, photovoltaic efficiency.

# 1. INTRODUCTION

The global rise of renewable energies has placed photovoltaic (PV) technologies at the heart of the energy transition. Owing to its technological maturity, scalability, and continuous cost reduction, crystalline silicon (c-Si) remains the dominant material, accounting for over 90 % of all solar cells produced worldwide [1, 2]. However, single-junction cells are approaching their theoretical efficiency limit (~ 29 %), motivating the development of advanced architectures such as silicon heterojunction (SHJ) devices that combine hydrogenated amorphous silicon (a-Si:H) with crystalline silicon (c-Si) [1-4].

SHJ cells exhibit high conversion efficiencies (> 26 %), low-temperature fabrication, and excellent operational stability. Their symmetrical structure, comprising intrinsic a-Si:H(i) passivation layers and doped selective contacts (p⁺/n⁺-a-Si:H), reduces surface recombination and improves carrier transport [1,3,4-6]. Yet, the overall performance strongly depends on the opto-electronic properties of the doped front and rear layers (FSF and BSF), whose thickness and doping concentration directly influence the field passivation, series resistance, and carrier collection [3,7].

Among these layers, the Back-Surface Field (BSF) plays a crucial role by limiting rear-surface recombination and creating an electric field that drives minority carriers toward the junction [3,7,8]. An optimized BSF must thus combine high conductivity to minimize ohmic losses with effective passivation to reduce the reverse saturation current. Achieving the right balance between these competing effects depends strongly on the doping level and thickness of this layer [3,7,8,9,10].

In this work, we present a comprehensive numerical modeling study using TCAD SILVACO-ATLAS of a double-heterojunction a-Si:H(n⁺)/c-Si(n)/a-Si:H(p⁺) solar cell. The goal is to quantify the combined influence of BSF thickness and doping on the main photovoltaic parameters: the open-circuit voltage (Voc​), short-circuit current density (Jsc​), fill factor (FF), and conversion efficiency (η).

This analysis aims to identify the optimal rear-layer configuration and provide physical insight into recombination and transport mechanisms, thereby guiding the design of high-efficiency, cost-effective SHJ solar cells [11].

2. METHODLOGY

# ELECTRICAL MODELING AND SIMULATION OF A SOLAR CELL

## 2.1. Modeling

The electro-optoelectronic behavior of a photovoltaic (PV) cell is classically described by a two-diode equivalent circuit complemented by

- a light-generated current source Iph and

- series Rs and shunt Rsh resistances.

This framework links junction physics (diffusion and generation–recombination) to the measured I-V curve and serves as the reference tool for parameter extraction and for simulating PV modules and arrays [12–14].

- Photogenerated source Iph: set by irradiance, spectrum, and temperature (through the EQE and optical losses) [12].

- Two diodes: D1 (ideality factor n1≈1) accounts for diffusion in quasi-neutral regions; D2 (n2≈2) accounts for generation–recombination in the space-charge region [13,14].

- Parasitic losses: Rs aggregates ohmic drops (contacts, metallization, TCO), while Rsh models leakage (defects, edges, parasitic paths) [13,14].

Its operation can be represented by the equivalent electrical circuit shown in Figure 1, whose parameters are experimentally determined using the current–voltage characteristic.

Figure 1: equivalent electrical circuit of a photovoltaic solar cell

By applying nodal analysis to the circuit, the output current of the cell is:

I=Iph-ID1-ID2-ISh                                                                                   (1)

With:

- I: cell output current (A).

- Iph: photogenerated current (A).

- ID1, ID2: diode currents (diffusion for D1; SRH in SCR for D2) (A).

- Ish: shunt current (A).

ID1=I01expqV+IRSn1KT-1                                                            (2)

ID2=I02expqV+IRSn2KT-1                                                            (3)

Ish=V+IRSRsh                                                                              (4)

I=Iph-I01expqV+IRSKT-1-I02expqV+IRS2KT-1-V+RSIRsh            (5)

Where:

- I01 ,I02: saturation currents (A);

- V: terminal voltage (V);

- Rs: series resistance (Ω);

- n1, n2: ideality factors;

- q: elementary charge (C);

- k: Boltzmann constant (J K-1);

- T: temperature (K).

- Rsh: shunt resistance (Ω).

This formulation avoids mixing currents and current densities (a frequent source of inconsistencies) and aligns with the five-parameter models used under real-world conditions [12,13].

Parameterization and key physical effects.

- Temperature: J0i increases strongly with T, degrading Voc; thermal laws (bandgap, mobilities, resistivities) are included [12].

- Spectrum/irradiance: Jph is quasi-linear with irradiance but spectrum-dependent (EQE). The efficiency tables (2025) confirm the advantage of passivating contacts for high Voc and FF [2].

- Passivating contacts & SHJ: interface passivation and selective contacts lower J02 and improve Rsh, yielding gains in Voc and fill factor; recent reviews summarize these advances [1,5,6], and 2024–2025 studies show industrial improvements [15].

## 2.2. Electrical performance parameters of a photovoltaic cell

Under illumination, the current–voltage relation of a cell (or module) is read from the I-V curve, from which the key figures of merit are extracted: short-circuit current Isc (or current density Jsc), open-circuit voltage Voc, fill factor FF, and efficiency η [1,2,12].

### 2.2.1. Short-circuit current Isc

At zero voltage (V=0), the delivered current reaches its maximum (short circuit). In the two-diode model, if resistive losses are small (Rs→0, Rsh→∞), one obtains

Isc​≈Iph                                                                            6

Isc: short-circuit current (A), proportional to irradiance and spectrum; in density form, Jsc=Isc/A  (A m-2).

Iph: photocurrent generated by light (A).

Remark: Eq. (5) is the standard approximation in the limit Rs→0, Rsh→∞. In practice, Isc deviates from Iph if Rs or recombination increases [12,16].

### 2.2.2. Open-circuit voltage Voc

At zero current (I=0), the maximum voltage is

Voc=nKTq.ln Iph I0+1                                                                (7)

With:

n: diode ideality factor (≈ 1 for diffusion; ≈ 2 for G–R in the SCR).

k: Boltzmann constant 1.38×10-23 (JK-1).

T: absolute temperature (K).

q: elementary charge 1.602×10-19 (C).

I0: (dark) saturation current of the diode (A).

VT​=kT/q: thermal voltage (≈ 25.85 mV at 300 K).

Note: Eq. (6) follows from the Shockley equation applied to PV cells; Voc​ grows roughly log-linearly with Iph​ and decreases with temperature [12,16].

### 2.1.3. Instantaneous power

The electrical power delivered is the product of voltage and current:

PW :V.I                                                                                 (8)

P: power at the cell/module terminals (W)

V: measured voltage (V)

I: measured current (A).

### 2.1.4. Fill factor (FF)

The fill factor measures the “rectangularity” of the I-V curve:

FF=PmaxVoc.Isc×100                                                                         (9)

Pmax: maximum extractable power (W).

Voc: open-circuit voltage (V).

Isc: short-circuit current (A).

Useful approximations. For a near-ideal cell (low Rs, high Rsh), empirical relations link FF to Voc, e.g., Green (1981) via voc=Voc/(nVT​); such formulas and their modern refinements aid process control and quality assurance [17, 18].

At the maximum power point (MPP) (Vmp, Imp), one has

Pmax= Vmax. Imax                                                                (10)

Vmp: voltage at MPP (V).

Imp: current at MPP (A).

### 2.1.5. Conversion efficiency η

Efficiency is the fraction of incident optical power converted to electricity:

η=PmaxGA×100=FF.Voc.IscGA×100                                               (11)

with:

G: irradiance (incident power density) (W m-2).

A: device active area (m2).

Practice: η is reported at STC and tracked under real conditions using I-V translation procedures (e.g., IEC 60891:2021); recent evaluations compare and refine these procedures [19,20].

# 3. SIMULATION DETAILS AND DESCRIPTION OF THE DOUBLE-HETEROJUNCTION SOLAR CELL

The PV solar cell considered in this study is based on n-type crystalline silicon. It consists of four successive layers. The crystalline-silicon (c-Si) n-doped substrate ensures charge-carrier generation, while the front hydrogenated amorphous silicon (a-Si:H) emitter reduces interface defects. A transparent conducting oxide (ITO) layer is deposited on the emitter, forming the window layer; it serves as an optical window for incoming light while providing electrical conduction. Finally, the rear hydrogenated amorphous silicon layer (BSF: Back Surface Field) limits carrier recombination to improve the overall efficiency.

This baseline configuration is defined in the ATLAS simulator of the TCAD-SILVACO software [11], with the simulation parameters summarized in Table 1. Using the TCAD-SILVACO simulator requires entering the parameters of each material composing the solar-cell structure under study.

Table 1 : Material parameters used in the simulation

| Different later Physical characteristics | FSF (a-Si:H) | BSF (a-Si:H) | Substrate (c-Si) | Units |
| --- | --- | --- | --- | --- |
| D | 0.01 | 0.01 | 250 | μm |
| Eg | 1.7 | 1.7 | 1.12 | eV |
| χ | 3.9 | 3.9 | 4.05 | eV |
| τn | 1.10-6 | 1.10-6 | 1.10-3 | s |
| τp | 1.10-6 | 1.10-6 | 1.10-3 | s |
| μn | 1 | 1 | 1350 | cm2/V.s |
| μp | 0.5 | 0.5 | 450 | cm2/V.s |
| Nc | 2.1020 | 2.1020 | 2.8 1019 | cm-3 |
| Nv | 2.1020 | 2.1020 | 1.04 1019 | cm-3 |
| ε | 11.9 | 11.9 | 11.9 | F/cm |

With: D: layer thickness. Eg: bandgap. χ: electron affinity. ε: dielectric constant. NC: effective density of states for electrons in the conduction band. NV: effective density of states for holes in the valence band. μn: electron mobility. μp: hole mobility. τn,τp: electron and hole lifetimes.

The defects present in the two thin hydrogenated amorphous-silicon layers (rear BSF and variable for the front emitter) are listed in Table 2 below.

Table 2 : Defect-state densities and capture cross-sections in a-Si:H [21,22]

| Defect density | Values of defect density A | Values of defect density D | Units |
| --- | --- | --- | --- |
| NGA, NGD | 1,5.1015 | 1,5.1015 | cm-3 |
| NTA, NTD | 1.1021 | 1.1021 | cm-3 |
| EGA, EGD | 0,62 | 0.78 | eV |
| WGA, WGD | 0,15 | 0.15 | eV |
| WTA, WTD | 0.033 | 0.049 | eV |
| σn | 1.10-17 | 1.10-15 | cm-2 |
| σP | 1.10-15 | 1.10-17 | cm-2 |

NGA, NGD: densities of Gaussian-shaped acceptor and donor states, respectively.

NTA, NTD: densities of acceptor and donor states at the band edges.

EGA, EGD: energy of the Gaussian peak.

WGA, WGD: width of the distribution.

WTA, WTD: width of the tail distribution.

σn, σP: capture cross section for electrons and holes, respectively.

Figure 2 illustrates the classical architecture of a heterojunction photovoltaic solar cell. The different constituent layers responsible for converting light into electricity can be distinguished.

Figure 2: Schematic diagram of a heterojunction PV solar cell.

All simulations of the heterojunction PV solar cell were carried out under standard operating conditions: AM1.5 spectrum, light intensity of 0.1 W/cm², and temperature of 300 K [23, 24].

# 4. RESULTS AND DISCUSSION

The study of the geometric and physical parameters on the opto-electrical characteristics (efficiency, open-circuit voltage, current density, and fill factor) of the BSF layer of a heterojunction PV solar cell makes it possible to determine the optimal geometry of the rear side as well as its doping level.

In this part, we investigate the effect of the BSF layer thickness on the performance of the PV solar cell using the ATLAS simulator of the TCAD-SILVACO software. The two key parameters of the rear hydrogenated amorphous silicon layer (n⁺-a-Si:H), namely its thickness and its doping level, are studied as the main variables.

First, we varied the thickness of the BSF layer from 2 nm to 20 nm for different values of the base thickness, while keeping the dopant concentration constant as well as the other physical parameters of the device. Second, we varied the doping level of this same layer, the BSF, while keeping those of the others fixed.

## 4.1. Effect of BSF (Back Surface Field) thickness on PV parameters

The BSF layer (Back Surface Field: (n⁺)-a-Si:H) is generally heavily doped and has the same doping type as the substrate. It is a decisive layer in the overall performance (efficiency, current density, open-circuit voltage, and fill factor) of a silicon heterojunction PV cell. It is intended to reduce minority-carrier recombination at the rear side and to facilitate their motion toward the junction. In what follows, we simulate a PV solar cell with several substrate thicknesses by varying the thickness of the BSF layer.

### 4.1.1. Effect of BSF thickness on the efficiency of the PV cell

Figure 3 shows the evolution of efficiency as a function of the variation of the rear-layer thickness of a heterojunction PV solar cell, for different substrate thicknesses.

Figure 3: Evolution of efficiency as a function of BSF thickness and for different values of the base thickness.

The analysis of Figure 3 indicates that the efficiency of the PV solar cell is proportional to the substrate thickness. It also shows a similar trend in efficiency for different PV cells with varied substrate thicknesses. The efficiency of the PV cell remains unchanged for a BSF layer thickness between 2 and 5 nm. By contrast, it increases very slightly by 0.04% in absolute value when the BSF thickness increases from 5 to 10 nm. The maximum efficiency is found when the BSF layer thickness lies between 10 nm and 13 nm, before it degrades beyond a thickness greater than 13 nm.

Indeed, a thin BSF layer (2 to 5 nm) allows losses due to rear-side recombination to persist. Conversely, an optimal thickness between 10 nm and 13 nm leads to good passivation and to the emergence of a electric field created by the heterojunction, crystalline silicon / hydrogenated amorphous silicon (c-Si/a-Si:H), which repels minority charges and thus reduces recombination. As a result, the efficiency produced by the PV solar cell increases [3, 7]. The thickness of the BSF layer must be well optimized. If the layer is too thin, it does not effectively block recombination through passivation. On the other hand, if it is too thick, it leads to an increase in resistive losses [3,7,25].

### 4.1.2. Effect of BSF thickness on the short-circuit current density of the PV cell

The short-circuit current density Jsc quantifies the fraction of photogenerated carriers actually collected at V=0. It reflects a trade-off between optics (c-Si absorption, reflection/ITO/a-Si:H losses) and electrical factors (surface/volume recombination, rear-contact selectivity).

Figure 4 highlights the evolution of the short-circuit current density as a function of the variation in the thickness of the rear layer of a heterojunction PV solar cell, for different substrate thicknesses.

Figure 4: Evolution of current density as a function of BSF thickness and for different values of the base thickness

Analysis of Figure 4 shows that the short-circuit current density is inversely proportional to the substrate thickness. The behavior of the current density is not linear. Figure 4 also shows that this current density evolves very slowly for a BSF layer thickness:

- 2-5 nm: Jsc changes very little; rear-surface passivation remains insufficient, so recombination losses persist.

- 5-10 nm: Jsc reaches a maximum thanks to improved interface passivation and field-effect selectivity at the rear contact, typical for SHJ stacks near a few-nanometer optimum [1,3,7].

- > 10 nm: a slight decrease appears (≈ 0.21 mA·cm-2 from 10 to 20 nm in our simulations) due to higher contact resistivity in doped a-Si:H and increased parasitic absorption; overall collection is penalized [1,3].

Substrate-thickness note.

Saying Jsc is “inversely proportional” to wafer thickness is not general: for a given optical stack, a thicker wafer increases the effective optical path and tends to raise Jsc (until saturation). If Fig. 4 shows the opposite, it likely reflects lifetime/recombination settings unfavorable to thicker wafers, insufficient rear reflectance, or an optical design (no texturing/mirror) disadvantaging thicker samples, trade-offs widely reported for SHJ [3,7,4,25].

Practical takeaway.

- BSF window: 5-10 nm, tuned with doping/anneal/TCO.

- Above that, monitor contact resistivity and optical losses.

- Co-optimize optics (AR, texturing, rear mirror) and passivation to preserve Jsc​ when adjusting BSF thickness [3,25].

### 4.1.3. Effect of BSF thickness on the fill factor (FF) of the PV cell

Figure 5 presents the trend of the fill factor (FF) as a function of the variation in the thickness of the rear layer of a heterojunction PV solar cell, for different substrate thicknesses.

Figure 5: Evolution of the fill factor as a function of BSF thickness and for different values of the base thickness.

Observed trends.

- In your simulations, thicker wafers exhibit lower FF. This is not universal; in principle, FF is mainly driven by Rs, Rsh, diode parameters (via voc), and recombination losses. The apparent thickness effect here reflects the chosen optical/recombination settings [2,5,6].

- As BSF thickness increases from 2 nm to 20 nm, FF rises markedly (from 38.40% to 83.16%), consistent with reduced rear recombination (lower effective J02, higher Voc) and stronger carrier selectivity, yielding a more rectangular I-V curve [1,3,7].

- Typically, very thick doped a-Si:H can increase Rs and eventually cap or reduce FF; your monotonic rise up to 20 nm indicates that recombination reduction still dominates, or that Rs is limited elsewhere (TCO/contacts) in this setup [3,17, 18].

Physical interpretation

- Very thin BSF (≈ 2-5 nm): incomplete passivation which leads to high rear recombination which leads to less rectangular I-V result in low FF [3,16].

- Moderate thickening (≈ 5-15+ nm): a stronger electric field at the BSF and better passivation reduce rear recombination, improve the differential slope near MPP, and raise FF [13,7].

- Excessive thickness: risk of higher Rs and optical losses, which can ultimately limit or reverse FF gains [3,17,18].

Note on substrate thickness

The observation “FF decreases with increasing wafer thickness” is not a general rule. To isolate causes, you can:

- keep Rs​ and Rsh​ fixed while sweeping wafer thickness,

- enforce identical optical conditions (same AR coating, texturing, rear mirror), and

- compare FF using FF vs voc​ empirical relations to separate recombination effects from resistive effects [17,18].

Takeaway

- In your dataset, thickening the BSF from 2 to 20 nm yields a strong FF improvement (38.40% → 83.16%).

- For broader generality, watch for a potential optimum if Rs​ begins to dominate at larger thickness, and consider an FF-voc analysis for robust benchmarking [17,18].

### 4.1.4. Effect of BSF thickness on the open-circuit voltage of the PV cell

Figure 6 displays the evolution of the open-circuit voltage Voc versus rear n+-a-Si:H BSF thickness, for several crystalline-silicon substrate thicknesses.

Figure 6: Evolution of the open-circuit voltage as a function of BSF thickness and for different base thickness values.

Observed trends (Fig. 6)

- In these simulations, Voc​ decreases as the wafer thickness increases. This is not universal: from the standard relation (see Eq. (6)),

Voc=nkTqlnIphI0+1

- Voc is governed by the effective saturation current I0 (volume/surface recombination) and by Iph [2]. An apparent thickness dependence typically reflects recombination settings (lifetimes, rear passivation) and/or optical conditions specific to the case studied [1,3,7].

- Conversely, increasing BSF thickness from 2 to 20 nm yields a slight rise in Voc (from 0.728 V to 0.729 V), consistent with reduced rear-surface recombination, i.e., a lower effective I0 thanks to improved passivation/selectivity at the rear contact [1,3,7].

- Beyond a certain BSF thickness, the Voc gain saturates: a very thick doped layer no longer significantly reduces I0 and may increase Rs or optical losses (not directly changing Voc in the quasi-static sense, but coupled to I-V shape) [3,7,17,18].

Takeaway

- In your data, thickening the BSF from 2 → 20 nm yields a small but positive Voc increase (+1 mV), consistent with lower rear recombination.

- The apparent dependence on wafer thickness mainly reflects recombination/optical settings in this simulation; to isolate effects, keep recombination parameters constant and compare under identical optics (AR, texturing, mirror) [1,3,7,25].

## 4.2. Influence of BSF doping on PV parameters

The BSF (n+-a-Si:H) critically governs SHJ performance: its doping sets:

- carrier selectivity and field-effect passivation at the rear,

- contact conductivity (thus Rs), and

- the defect density level correlated with high doping in a-Si:H.

In this study, the BSF doping is swept from 1×1016 to 1×1020 cm-3 in regular steps under identical conditions (AM1.5G, T=300 K). We monitor η, Voc, Jsc, and FF [1,3,7,25].

### 4.2.1. Effet du dopage du BSF sur l’efficacité de la cellule PV

Figure 7 shows the efficiency trend as a function of the BSF layer thickness variation in a heterojunction PV solar cell with different substrate thicknesses.

Figure 7: Efficiency as a function of BSF doping for different base thickness

As BSF doping increases from 1×1016 to 1×1020 cm-3, cell efficiency rises from 23.24% to 24.05%. This clear yet moderate gain is attributed to:

- lower rear-surface recombination thanks to stronger carrier selectivity and electric-field passivation at the BSF (reduced effective I0​, slight increase in Voc​);

- reduced local series resistance at the rear contact due to higher conductivity in doped n+-a-Si:H, which improves FF (a more rectangular I-V curve) [3,17,18].

Physical picture.

- Low doping (≲1017 cm-3): limited selectivity leading to insufficient field-effect passivation, which increases rear recombination therefore reduces Voc and FF [1,3].

- Intermediate–high doping (1018-1020 cm-3) creates a stronger barrier for holes (minority at the n side) and improves conduction for electrons (majority) conduction, thereby decreasing I0 slightly increasing Voc increasing FF, and thus boosting η [3,7,17,18].

- Very high doping (beyond the practical optimum) introduces higher defect densities in doped a-Si:H, added optical losses, and/or unwanted tunnelling, so the efficiency saturates or even rolls off if Rs or defect-assisted recombination increases [1,3,7].

Practical takeaway.

BSF doping is a fine-tuning knob that must be co-optimized with layer thickness, interface passivation quality, and the TCO/metal stack to raise Voc and FF without hurting Jsc​ via optics. An FF-voc analysis (Green; Leilaeioun & Holman) helps separate recombination-driven from resistive gains in η [17,18,25].

### 4.2.2. Effect of BSF doping on the short-circuit current density of the PV cell

Figure 8 shows how the short-circuit current density Jsc varies with the doping of the rear n+-a-Si:H BSF for different wafer thicknesses.

Figure 8: Evolution of short-circuit current density as a function of BSF doping

Observed trends (Fig. 8)

As BSF doping increases, Jsc improves slightly: in your data, from 38.41 to 38.49 mA·cm-2 (gain ≈ +0.08 mA·cm-2).

This small yet consistent gain stems from a stronger rear electric field and better carrier selectivity, which push minority carriers (holes on the n-type side) away from the rear interface and reduce recombination prior to collection [3,7,8].

Higher doping also increases n+-a-Si:H conductivity, easing transport near the rear contact; still, the impact on Jsc is limited because Jsc is dictated primarily by optics (absorption/EQE) and recombination, rather than by purely ohmic transport [3,23].

Cautionary notes

At very high doping, risks include higher defect densities in doped a-Si:H, added optical parasitics, or unwanted tunneling, which may cancel the Jsc gain or even reverse it [21-22].

To isolate the electrical effect of doping on Jsc, keep constant:

- the optical stack (AR, texturing, rear mirror),

- lifetimes and surface velocities at front/rear, and

- the BSF thickness; then compare EQE and integrated Jsc [23].

Takeaway.
Increasing BSF doping strengthens field-effect passivation and selectivity, yielding a slight Jsc uplift (here ~+0.08 mA·cm-2). Optimization must be co-optimized with BSF thickness and optics to avoid adverse effects at very high doping [1,3,7,25].

### 4.2.3. Effect of BSF doping on the fill factor (FF) of the PV cell

Figure 9 presents the trend of the fill factor (FF) as a function of the doping level of the rear n+-a-Si:H BSF in a silicon heterojunction (SHJ) PV cell, for different wafer thicknesses.

Figure 9: Evolution of the fill factor as a function of BSF doping for different base thickness

Observed trends (Fig. 9)

- Increasing the BSF doping from 1×1016 to 1×1020 cm-3 produces a small but consistent improvement in FF, from 83.05% to 83.15% (+0.10 percentage point).

- This positive evolution indicates that, over this range, the benefits of stronger rear passivation and carrier selectivity still outweigh any adverse increase in transport/resistive penalties at the rear contact.

Physical interpretation

- A more heavily doped n+-a-Si:H BSF strengthens the electric field at the rear interface (field-effect passivation) and enhances carrier selectivity for electrons while repelling minority holes away from the rear, thereby reducing recombination prior to collection [1,3,7].

- At the same time, higher doping increases the conductivity of the doped a-Si:H and typically reduces the local series resistance at the rear contact. The combination of lower recombination (which tends to raise Voc​ slightly and improve the differential slope near MPP) and lower Rs​ leads to a more rectangular I-V curve and hence a higher FF [3,17,18].

- In terms of standard metrics, tracking FF as a function of voc=Voc/(nVT) helps confirm that the measured improvement is consistent with reduced recombination and controlled series resistance, in line with analytical/empirical relations reported in the literature [17,18].

Limits and practical cautions

- At very high doping, counter-effects may emerge:

- higher defect densities in doped a-Si:H can increase recombination;

- tunneling/barrier inhomogeneity may degrade RshR_{sh}Rsh​; and

- minor optical parasitics can accumulate.

In such cases, the FF gain may saturate or even reverse if Rs​ or Rsh are compromised [3,17,18].

- Therefore, BSF doping should be co-optimized with BSF thickness, front/back passivation quality, and the TCO/metal stack, and assessed under identical optical conditions to isolate the purely electrical impact. For benchmarking, an FF-voc​ plot is recommended to separate recombination-driven from resistive contributions [1,3,7,17,18,25].

Takeaway

Within the studied range, raising BSF doping yields a modest, reproducible increase in FF (83.05% → 83.15%). The trend is physically consistent with stronger field-effect passivation, better carrier selectivity, and lower rear-contact Rs. To generalize beyond this window, maintain a joint optimization of doping, BSF thickness, interface passivation, and contact stack, and verify performance using FF vs voc diagnostics [1,3,7,17,18,25].

### 4.2.4. Effect of BSF doping on the open-circuit voltage of the PV cell

Figure 10 shows the evolution of the open-circuit voltage Voc as a function of the doping of the rear n+-a-Si:H BSF, for different wafer thicknesses.

Figure 10: Evolution of the open-circuit voltage as a function of BSF doping for different base thickness

Observed trends (Fig. 10)

Increasing BSF doping from 1×1016 to 1×1020 cm-3 yields a modest rise in Voc​ from 0.728 V to 0.736 V (+8 mV). This behavior agrees with

Voc=nkTqlnIphI0+1

where a lower effective saturation current I0, due to stronger rear-surface passivation and higher carrier selectivity, increases Voc​ [3,7,16,18]. The gain is small because Voc​ depends logarithmically on I0​.

Physical picture

- Low → mid doping: limited selectivity increasing rear recombination thereby raising I0, lower Voc [3,7]​.

- Higher doping (within the optimal window): stronger electric-field passivation at the BSF and improves selectivity thereby decreasing I0​ decreases, Voc​ increases slightly [3,7,18].

- Very high doping: beware of defect-related recombination, tunneling, or barrier inhomogeneity, which can saturate or limit Voc​ improvements [3,7].

Practical note and metrology

The +8 mV increase in Voc​ contributes marginally to efficiency and complements FF improvements. For reliable comparison, measure under standard conditions (AM1.5G, STC) and apply I-V translation procedures where needed, to isolate the doping effect from test conditions [19,20,25].

# 5. CONCLUSION

The numerical study carried out using TCAD SILVACO-ATLAS enabled the modeling and optimization of the electrical behavior of a double-heterojunction solar cell based on hydrogenated amorphous and crystalline silicon.

The analysis focused on the influence of both the thickness and doping of the Back Surface Field (BSF) layer on the cell’s optoelectronic performance, specifically on the main parameters: open-circuit voltage Voc​, short-circuit current density Jsc​, fill factor FF, and overall efficiency η [12,16].

Simulation results reveal that:

- an optimal BSF thickness between 10 and 13 nm provides the best trade-off between rear-side passivation and series resistance penalties, consistent with SHJ literature on few-nanometer a-Si:H layers [3, 7, 8, 9, 10];

- a too thin BSF (2-5 nm) still allows significant recombination, while a too thick layer (>15 nm) increases ohmic losses, reducing overall gains [3, 7, 9, 10];

- increasing BSF doping from 1×1016 to 1×1020 cm-3 improves overall performance by reducing the reverse saturation current and rear recombination, leading to a slight increase in Voc​ (from 0.728 to 0.736 V), a stable Jsc​, and a slight rise in FF (from 83.05% to 83.15%).
These improvements result in a maximum efficiency of about 24.05% for the best configurations.

Hence, a heavily doped and optimally thin BSF proves crucial to enhancing carrier collection, rear passivation, and electrical stability of SHJ cells. The findings are in good agreement with recent experimental reports on high-efficiency silicon heterojunction devices [1-4,7,25].

For future work, the study can be extended to:

- the combined effect of doping, BSF thickness, and temperature,

- opto-thermal coupled modeling, and

- 3D carrier-transport simulations including interface traps and bulk defects.
Such developments would strengthen the understanding of efficiency-limiting mechanisms in SHJ cells and guide the design of ultrathin, high-performance heterojunction structures.

COMPETING INTERESTS DISCLAIMER:

Authors have declared that they have no known competing financial interests OR non-financial interests OR personal relationships that could have appeared to influence the work reported in this paper.

# REFERENCES

[1] S. De Wolf, A. Descoeudres, Z. C. Holman, and C. Ballif, (2012) “High-efficiency silicon heterojunction solar cells: A review,” Green, vol. 2, no. 1, pp. 7–24, DOI 10.1515/green-2011-0018

[2] M. A. Green, E. D. Dunlop, M. Yoshita, et al. (2025). “Solar cell efficiency tables (Version 66),” Progress in Photovoltaics: Research and Applications, vol. 33, e3919, https://doi.org/10.1002/pip.3919

[3] T. G. Allen, J. Bullock, X. Yang, A. Javey, and S. De Wolf, (2019). “Passivating contacts for crystalline silicon solar cells,” Nature Energy, vol. 4, pp. 914–928, https://doi.org/10.1038/s41560-019-0463-6

[4] H. Lin, M. Yang, X. Ru, et al. (2023). “Silicon heterojunction solar cells with up to 26.81% efficiency achieved by electrically optimized nanocrystalline-silicon hole contact layers,” Nature Energy, vol. 8, pp. 789–799, DOI:10.1038/s41560-023-01255-2

[5] B. Hoex, et al. (2024) “Passivating contacts for crystalline silicon solar cells: An evolving landscape,” Advanced Energy Materials, vol. 14, no. 15, 2304338, https://doi.org/10.1002/aenm.202304338

[6] Y. Zhang, T. Shi, L. Duan, B. Hoex, and Z. Tang, (2024). “Progress in passivating selective contacts for heterojunction silicon solar cells,” Nano Energy, vol. 131, 110282, https://doi.org/10.1016/j.nanoen.2024.110282

[7] H. Fujiwara and M. Kondo, (2007). “Effects of a-Si:H layer thicknesses on the performance of a-Si:H/c-Si heterojunction solar cells,” Journal of Applied Physics, vol. 101, no. 5, 054516, https://doi.org/10.1063/1.2559975

[8] A. Helmaoui, A. Belghachi, and B. Bellali, (2007) “Amélioration du rendement de collecte et la tension Voc d’une cellule solaire avec couche BSF,” Rev. des Énergies Renouvelables (CER’07, Oujda), pp. 153–156.

[9] A. Rawat and M. Sharma, “Numerical simulations for high-efficiency HIT solar cells using microcrystalline silicon as emitter and back surface field (BSF) layers, (2014).” Solar Energy, vol. 110, pp. 691–703, https://doi.org/10.1016/j.solener.2014.10.004 (EPAISSEUR BSF)

[10] M. N. Kateb, S. Tobbeche, and A. Merazga, “Influence of μc-Si:H tunnel recombination junction on the performance of a-Si:H/μc-Si:H tandem solar cell, (2017).” Optik, vol. 139, pp. 152–165. Available: https://www.sciencedirect.com/science/article/pii/S0030402617303649

https://doi.org/10.1016/j.ijleo.2017.03.099 (DOPAGE)

[11] ATLAS User’s Manual, Version 5.12.1, Silvaco Inc., Santa Clara, CA, USA.

[12] W. De Soto, S. A. Klein, and W. A. Beckman, “Improvement and validation of a model for photovoltaic arrays, (2006).” Solar Energy, vol. 80, no. 1, pp. 78–88, https://doi.org/10.1016/j.solener.2005.06.010 (INACCESSIBLE PRIVE)

[13] M. G. Villalva, J. R. Gazoli, and E. R. Filho, “Comprehensive approach to modeling and simulation of photovoltaic arrays, (2009). ” IEEE Transactions on Power Electronics, vol. 24, no. 5, pp. 1198–1208, DOI:10.1109/TPEL.2009.2013862 (COURANT TENSION)

[14] A. Bouraiou, M. Hamouda, A. Chaker, et al. (2015). “Modeling and simulation of photovoltaic module and array based on one and two diode model using MATLAB/Simulink,” Energy Procedia, vol. 74, pp. 864–877. https://doi.org/10.1016/j.egypro.2015.07.822 (COURANT TENSION)

[15] S. Ma, D. X. Du, C. Gao, et al., “Improving the performance of industrial TOPCon solar cells through the insertion of intrinsic a-Si layer, (2024). ” Solar Energy Materials & Solar Cells, vol. 275, 113024, https://doi.org/10.1016/j.solmat.2024.113024

[16] S. M. Sze and K. K. Ng. (2006). Physics of Semiconductor Devices, 3rd ed. Hoboken, NJ, USA: Wiley, https://doi.org/10.1002/0470068329 (LIVRE)

[17] M. A. Green, “Accuracy of analytical expressions for solar cell fill factor, (1981). ” Solid-State Electronics, vol. 24, pp. 788–789, https://doi.org/10.1016/0038-1101(81)90062-9

[18] M. Leilaeioun and Z. C. Holman, (2016). “Improved empirical relation between fill factor and open-circuit voltage,” Journal of Applied Physics, vol. 120, 123111, https://doi.org/10.1063/1.4962511

[19] B. Li, D. Diallo, A. Migan-Dubois, and C. Delpha, “On the evaluation and translation of I–V curves for PV modules,” Progress in Photovoltaics: Research and Applications, 2023, https://doi.org/10.1002/pip.3652

[20] M. Piliougine, P. Sánchez-Friera, and G. Spagnuolo, (2024). “Field performance assessment and I–V translation of PV modules,” Energies, vol. 17, no. 3, 566, https://doi.org/10.3390/en17030566

[21] M. J. Powell and S. C. Deane, (1993). “Improved defect-pool model for charged defects in amorphous silicon,” Physical Review B, vol. 48, pp. 10815–10827, doi: 10.1103/PhysRevB.48.10815.

[22] M. Rawa, et al., (2022). “Single-diode PV models and analytical/Lambert-W solutions: A review,” Sensors, vol. 22, 4173, doi: 10.3390/s22114173.

[23] ASTM G173-03(2020), Standard Tables for Reference Solar Spectral Irradiances: Direct Normal and Hemispherical on 37° Tilted Surface. West Conshohocken, PA, USA: ASTM International, doi: 10.1520/G0173-03R20.

[24] IEC 60904-3, Photovoltaic Devices — Part 3: Measurement Principles for Terrestrial Photovoltaic (PV) Solar Devices with Reference Spectral Irradiance Data (AM1.5). Geneva, Switzerland: IEC, Ed. 4 (2019). (No public DOI indicated.)

[25] H. Lin, et al., (2023). “Silicon heterojunction solar cells with up to 26.81% efficiency achieved by electrically optimized nanocrystalline-silicon hole contact layers,” Nature Energy, vol. 8, pp. 789–799, doi: 10.1038/s41560-023-01255-2.