COMPARATIVE EVALUATION OF SAPINDUS MUKUROSSI EXTRACT, 0.2% CHITOSAN AND 17% EDTA ON ROOT DENTINE  EROSION – AN IN-VITRO STUDY

Abstract:

Background:

Dental erosion refers to the chemical loss of tooth structure caused by acids or chelating agents. Chelators, when used in endodontic procedures, can induce demineralization of root canal walls. Prolonged contact of such agents with dentin not only facilitates the removal of the smear layer but also contributes to dentinal surface erosion

Aim:

This study aims to comparatively evaluate the effects of Sapindus mukorossi extract, 0.2% chitosan, and 17% EDTA on dentinal erosion.

Study Design: Invitro Study

Place and Duration of Study: Department of Conservative Dentistry and Endodontics, KVG dental college and hospital, Sullia India 574327, between November 2024 and December 2024.

Materials and Methods:

A total of sixty-four extracted human single-rooted maxillary and mandibular premolars were selected for this study. The teeth were randomly allocated into three experimental groups and one control group, each comprising 16 samples, as follows:

- Group I (n = 16): Ethanolic extract of Sapindus mukorossi

- Group II (n = 16): 0.2% Chitosan

- Group III (n = 16): 17% EDTA

- Group IV (n = 16): Distilled water (control)

The premolars were decoronated, and their root canals were chemo mechanically prepared using the respective irrigants. Subsequently, the instrumented canals were split longitudinally, and dentin blocks were obtained from the middle third of each root. These specimens were embedded in epoxy resin blocks, and dentinal erosion was assessed using a 3D profilometer. The data obtained were subjected to statistical analysis using ANOVA and the t-test.

Results:

EDTA demonstrated the highest mean erosion value, followed by Sapindus mukorossi and 0.2% chitosan . The differences among the groups were statistically significant, with            (p < 0.05).

Conclusion:

EDTA caused the greatest degree of root dentin erosion. Sapindus mukorossi extract and nano-chitosan demonstrated comparable erosive effects. These results indicate that the experimental irrigants could serve as potential alternatives to conventional agents, providing similar efficacy with possibly fewer adverse effects.

Keywords:

dentin erosion, sapindus mukkurosi , herbal irrigants

Introduction

Dental erosion refers to the pathologic, chronic loss of dental hard tissues due to the chemical influence of extrinsic and intrinsic acids, without the involvement of bacteria1. During endodontic procedures, chelating agents used for root canal instrumentation can induce chemical alterations in dentin, such as erosive changes, leading to a reduction in dentin microhardness.2 Among these, ethylenediaminetetraacetic acid (EDTA) is considered the gold standard chelating agent, particularly during the final irrigation protocol, often used in alternation with sodium hypochlorite (NaOCl). However, extended exposure to EDTA has been shown to abstract peritubular and intertubular dentin, which can adversely affect the dentin ultrastructure, mechanical strength, and surface roughness, thereby compromising the overall durability and sealing of the root canal filling3.  Chelating agents like EDTA are essential for removing the smear layer, which is a mix of organic and inorganic debris generated during instrumentation4. While EDTA effectively opens up the dentinal tubules for better penetration of disinfectants and sealers, prolonged exposure can result in erosion of the dentinal walls, making the tooth more susceptible to fracture. Sodium hypochlorite (NaOCl), on the other hand, is excellent at dissolving organic tissue but lacks the ability to remove inorganic material, which is why it is alternated with EDTA. The balance between effective cleaning and preserving dentin integrity is critical. Using EDTA for too long or at high concentrations can weaken the root structure by leaching out calcium and altering the collagen matrix.

Chitosan is a natural polysaccharide known for its excellent biocompatibility, antimicrobial, and chelating properties. When formulated as nanoparticles, chitosan offers enhanced surface area, improving its effectiveness in removing the smear layer, particularly in the apical third of the root canal. Compared to traditional chelating agents like EDTA, chitosan causes significantly less dentin erosion, thereby preserving the mechanical integrity of the dentinal structure5. It exhibits strong antibacterial activity, especially against Enterococcus faecalis, a microorganism commonly resistant to conventional irrigants. Furthermore, chitosan has minimal cytotoxicity, making it safer for periapical tissues in the event of extrusion. Its eco-friendly nature and potential for sustained release further support its use as a promising alternative irrigant in endodontic therapy.

Sapindus mukorossi, commonly known as soapnut, is a plant-derived extract rich in saponins and possesses natural surfactant properties. It has been shown to be effective in smear layer removal, with efficacy comparable to EDTA when used at optimal concentrations6. Unlike conventional chelating agents, S. mukorossi causes less dentin erosion, thereby helping to preserve dentin microhardness and surface integrity. It also exhibits mild antimicrobial activity and demonstrates good biocompatibility, making it a promising herbal alternative in endodontic irrigation. Due to its natural origin, it carries a reduced risk of cytotoxicity, allergic reactions, and environmental toxicity. These attributes make it particularly suitable for use in herbal irrigation protocols, especially within the scope of minimally invasive and regenerative endodontic procedures.

Hence the objective of the study is to compare and evaluate the effect of sapindus mukurossi extract, 0.2 % chitosan and 17 % EDTA on the root dentine erosion. null hypothesis was there was no statistically significant difference in the root dentinal erosion between the tested groups , sapindus mukurossi and chitosan.

Materials and methodology

Ethical Approval and Informed Consent

The approval to conduct the experimental in vitro study was obtained from the Ethics Committee of the Institutional Review Board. The study strictly adhered to the guiding principles of the Declaration of Helsinki to ensure ethical research conduct.

Inclusion Criteria

Human single‐rooted mandibular premolars that were intact, noncarious, and extracted for orthodontic reasons were chosen for the study. All teeth had <10° curvature and approximately the same dimensions.

Exclusion Criteria

Teeth with more than one canal, existing caries, cracks, open apices, and curvature of roots more than 10° were excluded

Preparation of Specimens

A total of sixty four single rooted maxillary and mandibular premolar teeth were collected from the Department of Oral and Maxillofacial Surgery, KVG Dental College and hospital which were extracted for orthodontic purpose. The teeth were cleaned and stored in physiological saline until further processing.

Decoronation of all teeth at the level of cemento enamel junction was done under water cooling using a diamond disc. After working length confirmation, the root apices were sealed with sticky wax. Root canal preparation were performed using Neo endo rotary files. In between each file, Irrigation was performed with 5ml of Normal saline solution.

The specimens were randomly divided into four groups (n = 16) based on the final irrigating solution used:

- Group I (n = 16): Ethanolic extract of Sapindus mukorossi (5 mg/5 mL), irrigated with 5 mL for 3 minutes

- Group II (n = 16): 0.2% Chitosan solution, irrigated with 5 mL for 3 minutes

- Group III (n = 16): 17% Ethylenediaminetetraacetic acid (EDTA), irrigated with 5 mL for 3 minutes

- Group IV (n = 16): Distilled water, irrigated with 5 mL for 3 minutes

Preparation of irrigants

A 0.2% chitosan acetate solution was prepared by dissolving 0.2 g of chitosan powder in 100 ml of 1% acetic acid. The mixture was continuously stirred for 2 hours using a magnetic stirrer until a clear and homogeneous solution was obtained. The solution was subsequently stored under refrigeration and utilized within one week of preparation.

The experimental root canal irrigant was prepared from the dried fruits of Sapindus mukorossi. The hard seed nut was carefully removed with a sharp knife, and the pericarps were reduced to a fine powder using a household blender. The powdered material was extracted twice with absolute ethanol (99%) for a duration of two weeks at room temperature. Following extraction, the mixture was filtered and the solvent was evaporated using a rotary evaporator. The resulting extract was stored in sterilized screw-capped vials at −20°C until further use. For experimental application, the preserved extract was re-dissolved in distilled water to obtain a working concentration of 5 mg/ml as an irrigant.

The irrigating solutions were dispensed using 31-gauge irrigating needle. Root canals were then dried using sterile paper points. All roots were sectioned longitudinally by making groove at nearly midline of both buccal and lingual aspects of the root surface using a low-speed diamond disk. Root segments were mounted horizontally with dentin surfaces exposed using auto polymerizing acrylic resin and further grounded smooth with a series of fine emery papers. The dentine erosions are visualized through a 3D profilometer The collected optical data are processed by the instrument’s software.

Statistical Analysis

Statistical comparison among the groups was performed using One-Way Analysis of Variance (ANOVA). The level of significance was set at P < 0.05. All analyses were performed using SPSS Software version 23 (IBM, Armonk, NY, USA).

Results

The study evaluated the dentinal erosions after treatment with experimental irrigants like sapindus mukurossi , chitosan and conventional irrigants like EDTA.

The mean dentinal erosion value for Sapindus mukurossi extract group was 0.1225 ± 0.05756 µm, with values ranging between 0.05 and 0.25 µm. The Chitosan group demonstrated a mean erosion of 0.1306 ± 0.05744 µm, also within the range of 0.05 to 0.25 µm. In comparison, the EDTA group exhibited the highest mean dentinal erosion (0.1438 ± 0.08350 µm), with a broader range (0.02 to 0.30 µm)

Table:1 shows the Descriptive values of dentinal erosion among the studied groups

| Table No. 1: Descriptive values of dentinal erosion among studied groups. |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Extracts | N | Minimum | Maximum | Mean | Std. Deviation | Variance | P-value* |
| Sapindus Mukurossi Extract | 16 | .05 | .25 | .1225 | .05756 | .003 | <0.001** |
| Chitosan | 16 | .05 | .25 | .1306 | .05744 | .003 |  |
| EDTA | 16 | .02 | .30 | .1438 | .08350 | .007 |  |
| Control | 16 | .01 | .08 | .0337 | .02125 | .000 |  |

Table No.2: Significance level of Pair wise comparison between the studied groups

| Extracts | Chitosan | EDTA | Control |
| --- | --- | --- | --- |
| Sapindus Mukurossi | 0.82 | 0.13 | 0.005** |
| Chitosan |  | 0.17 | <0.001** |
| EDTA |  |  | <0.001** |

Independent samples t test

**p value <0.05 was considered statistically significant.

Graph 1: Mean dentinal erosion among the studied groups.

Discussion

The effectiveness of root canal irrigation is largely determined by the ability of the solution to remove the smear layer and facilitate disinfection, while simultaneously preserving dentin integrity. An ideal irrigant should therefore balance antimicrobial activity with minimal adverse effects on the structural and chemical properties of dentin. However, commonly used solutions such as ethylenediaminetetraacetic acid (EDTA) are known to induce dentin demineralization and surface erosion, raising concerns regarding their long-term influence on root strength and treatment outcomes. The present study compared the erosive effects of Sapindus mukurossi extract, chitosan, and EDTA on root dentin, with a distilled water group serving as control. The findings provide insights into how these irrigants interact with dentin surfaces and contribute to the growing body of evidence on alternative chelating solutions in endodontics.

EDTA, which has a neutral pH, acts on intraradicular dentin primarily by replacing calcium ions in hydroxyapatite with hydrogen ions. This chelation process increases dentin surface roughness and, when used for prolonged periods (especially in contact times beyond 2–3 minutes), it can remove peritubular and intertubular dentin, reducing microhardness and increasing susceptibility to root fractures. Chitosan, on the other hand, is a weak chelating agent. Its amino groups interact with metal ions (notably calcium) via adsorption and ion exchange mechanisms, causing gradual depletion of inorganic components from the smear layer. This action, contributes to increased surface roughness, although to a lesser extent than EDTA. When used as nanoparticles, chitosan exhibits enhanced physicochemical properties—small size, hydrophilicity, and larger surface-area-to-volume ratio—which allows superior penetration into dentinal tubules and more efficient smear layer removal while minimizing dentin erosion7.  Chitosan nanoparticle formulations, typically prepared by dissolving chitin in acetic acid, have shown smear layer removal efficacy comparable to EDTA—achieving clean dentinal tubules in all thirds of the canal—with significantly less reduction in calcium/phosphorus ratio 8. Sapindus mukorossi (Indian soapnut) contains potent triterpenoid saponins that impart surfactant-like properties. In vitro studies have shown that its extracts effectively remove the smear layer without aggressively demineralizing dentin and can even dissolve pulp tissue, though less effectively than sodium hypochlorite. Its saponins reduce surface tension, enhancing smear layer cleaning, while maintaining dentin microhardness and structural integrity. Because it is plant-derived and biodegradable, the extract carries low cytotoxicity, minimal allergenic potential, and negligible environmental toxicity. The triterpenoid saponins in S. mukorossi decrease surface tension and emulsify organic debris, providing dual action in smear layer disruption and mild antimicrobial activity; some extracts have demonstrated limited pulp tissue dissolution, offering alternative clinical utility9.

Conclusion

Within the limitations of this study, it can be concluded that all tested irrigants produced measurable dentinal erosion, with EDTA showing the highest mean values. Both Sapindus mukurossi extract and chitosan demonstrated comparatively lower erosive potential, suggesting that they may serve as promising alternatives to conventional chelating agents. The control group exhibited minimal erosion, confirming the role of the irrigants in surface alterations.

.

### Limitations of the Study

Further in-depth investigations, including long-term in vivo studies, are warranted to validate these findings and to establish the clinical relevance of herbal and biopolymeric irrigants in endodontic therapy. The present investigation was conducted under in vitro conditions, which do not fully replicate the complex biological environment of the oral cavity. Factors such as the buffering action of dentinal fluid, presence of pulp tissue, and dynamic intraoral conditions were not simulated in this study. Additionally, only short-term effects of the irrigants on dentin erosion were evaluated, without assessing their long-term influence on structural integrity or clinical outcomes. The sample size, although adequate for preliminary analysis, may limit the generalizability of the results.

References

1.Ulusoy Öİ, Tunc ES, Bayrak S, Cebeci ARİ. Evaluation of mineral content in primary teeth with different treatments. Microsc Res Tech. 2012;75(9):1203–8.

2. Zehnder M. Root canal irrigants. J Endod. 2006;32(5):389–98.

3.  Aksel H, Serper A, Sahin C, Altundasar E. Evaluation of the effects of various irrigation protocols on the removal of triple antibiotic paste from simulated root canal irregularities. J Endod. 2016;42(9):1469–73.

4. Hemmat N, Vesal N, Dehghan S. Effect of different irrigation regimens on root canal dentin: a scanning electron microscopy and atomic force microscopy evaluation. Microsc Res Tech. 2020;83(1):84–91.

5. Aldo GM, Ferreira NS, Alves FRF, Almeida BM, Gomes BPFA. Chitosan: A natural antimicrobial agent in endodontics. Int Endod J. 2019;52(7):1107–22.

6. Tahir S, Mushtaq M, Farooq I, Al-Madi EM. Efficacy of Sapindus mukorossi extract as an endodontic irrigant in smear layer removal: An in vitro study. J Taibah Univ Med Sci. 2020;15(5):390–6.

7. Abdelkafy, Heba1; Elsheikh, Hemat Mostafa1; Kataia, Mohamed Medhat Efficacy of using chitosan and chitosan nanoparticles as final irrigating solutions on smear layer removal and mineral content of intraradicular dentin. Journal of Indian Society of Pedodontics and Preventive Dentistry 41(2): p 170-177, Apr–Jun 2023. | DOI: 10.4103/jisppd.jisppd_89_23

8.Güçlüer Ö, Akarsu E, Yavuz E, Er K, Kuştarcı A. Human pulp tissue dissolution ability of different extracts of Sapindus mukorossi: An in vitro study. Chin Herb Med. 2020 Mar 14;12(2):178-182. doi: 10.1016/j.chmed.2019.11.005. PMID: 36119798; PMCID: PMC9476676.