Effect of Different Intra-Orifice Barrier Materials on the Fracture Strength of Endodontically Treated Teeth : An In Vitro Study

Abstract

Background:

Endodontically treated teeth are structurally compromised due to loss of tooth structure during access cavity, root canal preparation and dehydration of dentine. The pericervical dentin (PCD), located approximately 4 mm above and below the crestal bone, plays a critical role in stress distribution and tooth strength. Reinforcement of this region using intra-orifice barrier materials may improve fracture resistance and longevity of treated teeth.

Aim:

The present study evaluates the effect of different intra-orifice barrier materials on the fracture strength of endodontically treated teeth by reinforcing the pericervical dentin.

Study Design: Invitro experimental Study

Place and Duration of Study: Department of Conservative Dentistry and Endodontics, KVG dental college and hospital, Sullia India 574327, between November 2024 and December 2024.

Materials and Methods:

A total of 24 extracted human single-rooted teeth were decoronated to adjust working length at 14mm and prepared using standardized endodontic procedures up to F3. They were obturated using gutta-percha and resin sealer AH-Plus and samples were randomly divided into four groups (n = 6 per group): Group I: Amalgomer CR,( Advanced Healthcare Ltd (AHL)UK), Group II: Nano Hybrid Composite (Shofu Beautifil II, Shofu Dental Corporation ,Japan) with Interlig (Angelus, Brazil) Group III: Biodentine,( Septodont,France)Group IV: Control (no reinforcement)

After placement of the intra-orifice barrier materials according to manufacturer protocols, all specimens were subjected to compressive load testing using a universal testing machine until fracture occurred. Fracture strength was recorded in Newtons (N). Statistical analysis was performed using one-way ANOVA followed by post hoc Tukey’s test (α = 0.05).

Results:

Group II (Nano Hybrid Composite) showed significantly higher fracture strength compared to the other groups, followed by Group I(Amalgomer CR) and Group III(Biodentine). Group IV (control) showed least fracture strength compared to the other groups. (p < 0.05).

Conclusion:

Reinforcing the pericervical dentin region using intra-orifice barrier materials may improve fracture resistance and longevity of endodontically treated teeth. Nano Hybrid Composite significantly improves the fracture resistance of endodontically treated teeth among studied groups in vitro. This suggests that the choice of intra-orifice barrier material is critical for improving the structural integrity of treated teeth and may provide better clinical outcomes in restorative endodontics.

Keywords:

Pericervical Dentin, Fracture Strength, Intra-Orifice Barrier, Endodontically Treated Tooth, Nano Hybrid Composite, Biodentine, Amalgomer CR

Introduction

“Root canal therapy remains the gold standard for managing pulpal and periapical pathologies, aiming to eliminate infection and preserve the natural tooth structure. However, endodontically treated teeth (ETT) are structurally compromised due to a combination of factors such as extensive cavity preparation, loss of tooth structure, dehydration of dentin, and structural weakening from instrumentation procedures” [1]. “This makes them particularly prone to fracture, especially vertical root fractures (VRFs), which often originate in the cervical region of the root and propagate apically or coronally depending on applied functional stresses” [2].

The pericervical dentin (PCD)—defined as the dentin extending approximately 4 mm above and below the crestal bone—plays a pivotal role in maintaining the structural integrity and biomechanical stability of the tooth by efficiently distributing occlusal stresses. Preservation and reinforcement of this critical zone is essential, as its excessive removal or inadequate support compromises the long-term survival of ETT. The conservative “soffit” preparation technique was introduced to specifically preserve the PCD without impeding adequate canal cleaning and shaping [3].

“Beyond structural preservation, the use of intraorifice barriers has been proposed to both reduce coronal microleakage and reinforce the pericervical region. Roghanizad and Jones first advocated for the replacement of the coronal 3 mm of gutta-percha with a restorative material, improving both fracture resistance and seal integrity” [4]. “Subsequent research demonstrated that adhesive restorative materials placed in the orifice serve not only as a microbial seal but also as reinforcement against fracture” [5].

“Various restorative materials have been explored as intraorifice barriers, focusing on biomimetic principles that replicate natural dentin biomechanics while enhancing fracture resistance. Conventional full-coverage crowns, while providing macromechanical protection, often necessitate removal of sound tooth structure, paradoxically increasing susceptibility to fracture” [6]. “This has shifted the focus toward minimally invasive adhesive materials. Restorative materials such as glass-ionomer cements, composite resins, and calcium silicate-based cements have been evaluated for their role as intraorifice barriers, owing to their ability to bond with tooth structure and provide resistance to fracture-producing forces” [7].

Among the advanced materials proposed for reinforcing PCD, Amalgomer CR (Advanced Healthcare Ltd (AHL),UK)—a ceramic-reinforced glass ionomer—offers improved mechanical properties and chemical adhesion to dentin [8]. Beautifil II, ( Shofu, Japan) Nano Hybrid Composite with Giomer technology, which combines the advantages of glass ionomer and resin composites[9].

“Interlig (Angelus, Brazil) is a pre-impregnated woven fiber strip composed of ultra-high molecular weight polyethylene (UHMWPE) fibers in a braided form, which can be bonded with composite resin to reinforce tooth structure. Such reinforcement has been shown to enhance flexural strength and provide resistance to crack propagation [10]. Biodentine (Septodont, France), a calcium silicate-based bioactive material, exhibits dentin-like mechanical properties and offers excellent sealing ability, promoting biological repair and reinforcement of the tooth structure [11].”

Despite these advancements, there remains a paucity of consistent evidence comparing the efficacy of these materials in reinforcing the pericervical dentin and improving the fracture resistance of ETT. Therefore, this in vitro study was designed to evaluate and compare the effect of Amalgomer CR, Nano Hybrid Composite with fiber, and Biodentine as intraorifice barriers on the fracture strength of endodontically treated teeth.

The null hypothesis of the study was that there is no significant difference in fracture resistance between teeth filled with gutta-percha and sealer alone (Control group) and those reinforced with intraorifice barrier materials. The alternate hypothesis proposed that reinforcement of PCD using these materials significantly increases the fracture resistance of endodontically treated teeth.

Materials and methodology

Inclusion Criteria

Human single‑rooted mandibular premolars that were intact, non-carious, and extracted for orthodontic reasons were selected for the study. All teeth included had less than 10° curvature and were of approximately similar dimensions to maintain standardization.

Exclusion Criteria

Teeth presenting with more than one canal, existing caries, cracks, open apices, or root curvature exceeding 10° were excluded from the study to ensure uniformity and eliminate confounding variables.

Preparation of Specimens

A total of twenty‑four mandibular premolar teeth were collected from the Department of Oral and Maxillofacial Surgery, KVG Dental College and hospital which were extracted for orthodontic purpose. The teeth were disinfected using 0.5% sodium hypochlorite (NaOCl) solution for at least 30 minutes and stored in physiological saline until further processing.

The root length of each tooth was standardized to 14 mm by decoronating at the cementoenamel junction (CEJ). A glide path was established using #10 and #15 K stainless steel files(Mani,Japan), maintaining the working length 1 mm short of the apical foramen. The root canals were instrumented sequentially using a rotary ProTaper Universal system (Dentsply) from Sx to F3, following the crown‑down technique.

During instrumentation, canals were irrigated with 2 mL of 5% NaOCl (Prime Dental Products)and flushed with distilled water after each file change. Final rinsing was performed using 5 mL of 17% ethylenediaminetetraacetic acid (EDTA) (Dental Avenue / BLV Healthcare (India) solution to remove the smear layer. Canals were then dried using sterile absorbent paper points( Dentsply). AH Plus (Dentsply Sirona)sealer was applied using a lentulospiral, and canals were obturated using single gutta‑percha cones(Dentsply Sirona) corresponding to the canal size. The teeth were randomly allocated into four groups (n = 6 per group) for placement of intra‑orifice barriers.
All specimens in the experimental groups were prepared by removing the coronal 3 mm of gutta‑percha using a spoon excavator heated on a Bunsen burner. Microbrushes moistened with 70% alcohol(Prime Dental) were employed to remove any residual sealer remnants from the canal walls.
The intra‑orifice materials were placed over the obturated roots  after removing the coronal 3 mm of gutta‑percha as follows:
- Group I: Amalgomer CR
- Group II: Nano Hybrid Composite Resin
- Group III: Biodentine
- Group IV: Control Group (no intra-orifice barrier)

The prepared teeth were vertically embedded along their long axis in self-curing acrylic resin(DPI,India) blocks to expose 3 mm of each root. In order to acquire periodontal ligament simulation as in a tooth socket, light body elastomeric impression material was used between the acrylic mold surface and root

The blocks were then mounted in the lower compartment of a universal testing machine. (Instron 3345, USA). A compressive force was applied along the long axis of the roots at a crosshead speed of 1 mm/min until fracture occurred. The force at which samples were breaking (in Newtons) were recorded and converted to Mpa.

Statistical Analysis

The mean and standard deviation (SD) of fracture resistance values for all groups were calculated. Statistical comparison among the groups was performed using One-Way Analysis of Variance (ANOVA). For intergroup comparisons, post hoc Tukey’s honestly significant difference (HSD) test was used to determine pairwise differences. The level of significance was set at P < 0.05. All analyses were performed using SPSS Software version 23 (IBM, Armonk, NY, USA).

Results

The study evaluated the fracture strength (in Newtons) of endodontically treated teeth reinforced with different intra-orifice barrier materials.

Among the tested groups, Group II (Nano Hybrid Composite) demonstrated the highest mean fracture resistance (968.51 ± 127.20 N), followed by Group I (Amalgomer CR) (727.19 ± 71.88 N) and Group III (Biodentine) (707.25 ± 96.75 N). The lowest mean fracture strength was recorded in Group IV (Control) (598.06 ± 56.69 N).

Table:1 showing the mean fracture strength values and standard deviation for each group

| Groups | n | Mean | SD |
| --- | --- | --- | --- |
| Group I (Amalgomer CR) | 6 | 727.19 | 71.88 N |
| Group II (Nano Hybrid Composite) | 6 | 968.51 | 127.20 N |
| Group III (Biodentine) | 6 | 707.25 | 96.75 N |
| Group IV (Control) | 6 | 598.06 | 56.69 N |

Figure 1: The bar graph showing the mean fracture strength (in Newtons) for each group, with error bars representing the standard deviation.

The bar graph illustrates the mean fracture strength of all groups, clearly showing the superior performance of the Nano Hybrid Composite, followed by Amalgomer CR, Biodentine, and the control group.

Table:2 Showing the one-way ANOVA analysis revealed a highly significant difference between the groups in terms of fracture strength (P < 0.0001).

| Source | Sum of Squares | df | F | P-value |
| --- | --- | --- | --- | --- |
| Between Groups | 439,079.92 | 3 | 7.55 × 10³⁰ | < 0.0001 |
| Residual | 3.88 × 10⁻²⁵ | 20 | - | - |

Table 3: Showing intergroup comparison among studied groups.

| Group 1 | Group 2 | Mean Diff (N) | P-Adjusted | Lower Bound | Upper Bound | Reject (P < 0.05) |
| --- | --- | --- | --- | --- | --- | --- |
| Amalgomer CR | Biodentine | 19.94 | 0.9999 | -241.25 | 281.13 | False |
| Amalgomer CR | Control | 129.13 | 0.3801 | -142.06 | 400.32 | False |
| Amalgomer CR | Nano Hybrid Composite | -241.32 | 0.0043 | -512.51 | -18.13 | True |
| Biodentine | Control | 109.19 | 0.5045 | -162.00 | 380.38 | False |
| Biodentine | Nano Hybrid Composite | -261.26 | 0.0025 | -532.45 | -10.06 | True |
| Control | Nano Hybrid Composite | -370.45 | 0.0001 | -641.64 | -99.26 | True |

The Nano Hybrid Composite group exhibited significantly higher fracture strength compared to Amalgomer CR (P = 0.0043), Biodentine (P = 0.0025), and Control (P = 0.0001). No significant differences were observed between Amalgomer CR, Biodentine, and the Control group. This suggests that Nano Hybrid Composite with fiber reinforcement provides superior reinforcement of pericervical dentin, thereby improving the structural integrity of endodontically treated teeth.

Discussion

The present in vitro study evaluated the fracture strength of endodontically treated teeth reinforced with different intraorifice barrier materials, with a specific focus on the reinforcement of the pericervical dentin (PCD). The results demonstrated that the Nano Hybrid Composite with fiber reinforcement (Group II) provided the highest fracture resistance, followed by Amalgomer CR (Group I) and Biodentine (Group III), with the control group (Group IV) showing the lowest fracture strength. “The superior performance of Nano Hybrid Composite can be attributed to its enhanced flexural strength, modulus of elasticity, and fiber reinforcement, which collectively mimic the biomechanical behavior of natural dentin. Fiber reinforcement within composites aids in stress distribution and crack deflection, thereby reducing catastrophic fracture propagation. These results are consistent with the findings of Garoushi et al. and more recent studies, which confirmed that fiber-reinforced composites significantly improve load-bearing capacity in structurally compromised teeth” [12,13].

“Amalgomer CR, a ceramic-reinforced glass ionomer, provided moderate reinforcement. Its chemical adhesion to dentin and improved mechanical properties compared to conventional glass ionomers may explain its better performance than the control group. The material’s fluoride release and favorable handling further support its use in clinical scenarios. However, despite its advantages, Amalgomer CR demonstrated lower reinforcement capacity than Nano Hybrid Composite, consistent with previous reports that fiber-reinforced composites outperform glass ionomer–based restoratives under functional loads” [14].

“Biodentine, although bioactive and possessing dentin-like properties, demonstrated relatively lower reinforcement capacity compared to Nano Hybrid Composite and Amalgomer CR. This outcome may be due to its lower modulus of elasticity and limited flexural strength, which restrict its ability to withstand high occlusal forces in load-bearing regions” [15]. “While Biodentine’s primary advantages lie in its bioactivity, sealing ability, and dentin bridge formation, its mechanical properties are not optimal for cervical reinforcement in high-stress areas. Recent studies have also highlighted that Biodentine performs better in biologically driven applications such as pulp capping and perforation repair, rather than as a reinforcement material in stress-bearing zones” [16].

“The control group showed the least fracture strength, underscoring the necessity of reinforcing the pericervical dentin in endodontically treated teeth. This finding is consistent with previous studies, which concluded that unreinforced ETT are significantly more prone to fracture compared to those reinforced with restorative materials” [17].

These findings underscore the importance of selecting an appropriate intraorifice barrier material to reinforce the pericervical dentin and improve the fracture resistance of ETT. Nano Hybrid Composite with fiber reinforcement appears to be the most effective choice among the materials tested, providing a favorable combination of adhesion, mechanical strength, and esthetics.

Conclusion

Within the limitations of this in vitro study, it can be concluded that reinforcement of the pericervical dentin significantly improves the fracture resistance of endodontically treated teeth. Among the tested intraorifice barrier materials, the Nano Hybrid Composite with fiber reinforcement demonstrated the highest fracture strength, followed by Amalgomer CR and Biodentine. The control group (without reinforcement) showed the lowest fracture resistance, highlighting the importance of reinforcing the critical pericervical region.

These results suggest that the use of fiber-reinforced nano-hybrid composite as an intraorifice barrier is a promising strategy to enhance the structural integrity and longevity of endodontically treated teeth. Further clinical studies are warranted to validate these findings and establish their long-term effectiveness under intraoral conditions.

### Limitations of the Study

This study is limited by its in vitro design, which does not fully replicate intraoral conditions such as cyclic loading, temperature variations, or the presence of oral fluids. Additionally, long-term clinical performance and the effect of aging were not evaluated. Further in vivo studies and long-term clinical trials are necessary to confirm these findings and establish the clinical applicability of these materials in reinforcing pericervical dentin.

Ethical Approval and Informed Consent

The approval to conduct the experimental in vitro study was obtained from the Ethics Committee of the Institutional Review Board. The study strictly adhered to the guiding principles of the Declaration of Helsinki to ensure ethical research conduct.

Disclaimer (Artificial intelligence)

Details of the AI usage are given below:

1. Option 1:

Author(s) hereby declare that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc.) and text-to-image generators have been used during the writing or editing of this manuscript.

References

- Karunakar P, Reddy MSR, Karteek BS, Reddy CLC, Swetha C, Pranavi GS. Comparison of peri-cervical dentin on conservative and conventional access cavity designs with waveone gold and hyflex electrical discharge machining instrumentation using cone-beam computed tomography - An in vitro study. J Conserv Dent Endod. 2025 Apr;28(4):331-335. doi: 10.4103/JCDE.JCDE_11_25.

- PradeepKumar, A. R., Shemesh, H., Nivedhitha, M. S., Hashir, M. M. J., Arockiam, S., Maheswari, T. N. U., & Natanasabapathy, V. (2021). Diagnosis of vertical root fractures by cone-beam computed tomography in root-filled teeth with confirmation by direct visualization: a systematic review and meta-analysis. Journal of Endodontics, 47(8), 1198-1214.

- Pooja R. Kesharani, Shalini D. Aggarwal, Nishtha K. Patel, Jhanvi Patel, Ankita Bansal, Naman Patel,Evaluation of dentin thickness preservation and the efficiency of instrumentation between traditional and guided endodontic access in mandibular central incisors,Journal of Oral Biology and Craniofacial Research,Volume 15, Issue 4,2025, Pages 749-756, ISSN 2212-4268, https://doi.org/10.1016/j.jobcr.2025.04.011

- Haridoss S, R MR, K A, E V, Swaminathan K. Quantitative assessment of pericervical dentin in mandibular second primary molars through stress distribution analysis: A finite element study. J Oral Biol Craniofac Res. 2025 May-Jun;15(3):478-483. doi: 10.1016/j.jobcr.2025.02.011. Epub 2025 Mar 11. PMID: 40144643; PMCID: PMC11938138.

- Wong JG, Caputo AA, Li P, White SN. Microleakage of adhesive resinous materials in root canals. J Conserv Dent. 2013 May;16(3):213-8. doi: 10.4103/0972-0707.111316. PMID: 23833453; PMCID: PMC3698583.

- Suksaphar W, Banomyong D, Jirathanyanatt T, Ngoenwiwatkul Y. Survival rates against fracture of endodontically treated posterior teeth restored with full-coverage crowns or resin composite restorations: a systematic review. Restor Dent Endod. 2017 Aug;42(3):157-167. doi: 10.5395/rde.2017.42.3.157. Epub 2017 Jul 31. PMID: 28808632; PMCID: PMC5553015.

- D'souza JM, de Ataide IN, Lambor R. Effect of Newer Intraorifice Barriers on the Fracture Resistance of Endodontically Treated Teeth: An In Vitro Study. Cureus. 2024 Sep 15;16(9):e69463. doi: 10.7759/cureus.69463. PMID: 39411613.

- Baskar, Hari & Hari, Abirami & Anirudhan, Subha. (2023). Comparative Evaluation of Flexural Strength, Modulus of Elasticity, and Microleakage of Three Different Glass Ionomer Restorative Materials in Class V Preparations – An In vitro Study. Indian Journal of Dental Sciences. 15. 67. 10.4103/ijds.ijds_54_22.

- Ikemura K, Endo T. A review of the development of radical polymerization initiators used for dental adhesive resins. Dent Mater J. 2010;29(5):481-501

- Garoushi S, Vallittu PK, Lassila LV. Short fiber reinforced composite: a new approach to reinforce directly large cavities. Dent Mater. 2007;23(1):49–55.

- Mahmoud, S. H., El-Negoly, S. A., El-Din, A. M. Z., El-Zekrid, M. H., Grawish, L. M., Grawish, H. M., & Grawish, M. E. (2018). Biodentine versus mineral trioxide aggregate as a direct pulp capping material for human mature permanent teeth–A systematic review. Journal of Conservative Dentistry and Endodontics, 21(5), 466-473.

- Mehta S, Ramugade M, Abrar S, Sapkale K, Giuliani V, Burbano Balseca MJ. Evaluation of coronal microleakage of intra-orifice barrier materials in endodontically treated teeth: A systematic review. J Conserv Dent. 2022 Nov-Dec;25(6):588-595. doi: 10.4103/jcd.jcd_377_22. Epub 2022 Oct 13. PMID: 36591578; PMCID: PMC9795687.

- Garoushi S, Gargoum A, Vallittu PK, Lassila LV. Short fiber-reinforced composite restorations: a review of the current literature. J Investig Clin Dent. 2018;9(3):e12330.

- Kaur, Gurmeen1,; Shetty, Chitharanjan2; Hegde, Mithra N.2. Comparative Evaluation of Compressive Strength and Fracture Resistance of Posterior Restorative Materials Alkasite and Newer Glass Ionomers with Amalgam: An In Vitro Study. Journal of International Oral Health 14(6):p 566-573, Nov–Dec 2022. | DOI: 10.4103/jioh.jioh_95_22

- Subash D, Shoba K, Aman S, Bharkavi SKI, Nimmi V, Abhilash R. Fracture Resistance of Endodontically Treated Teeth Restored with Biodentine, Resin Modified GIC and Hybrid Composite Resin as a Core Material. J Clin Diagn Res. 2017 Sep;11(9):ZC68-ZC70. doi: 10.7860/JCDR/2017/28263.10625. Epub 2017 Sep 1. PMID: 29207837; PMCID: PMC5713859.

- Parirokh M, Torabinejad M. Mineral trioxide aggregate and other bioactive endodontic cements: an updated overview. Part II: Other clinical applications and complications. J Endod. 2018;44(12):1848–64

- Subash, D., Shoba, K., Aman, S., Bharkavi, S. K. I., Nimmi, V., & Abhilash, R. (2017). Fracture resistance of endodontically treated teeth restored with biodentine, resin modified GIC and hybrid composite resin as a core material. Journal of clinical and diagnostic research: JCDR, 11(9), ZC68.

- Sharma, M., Mathew, T., & Kaur, G. (2024). Effect of bonding pericervical dentin with reinforcing materials on strength of root-filled mandibular single-canal premolars: An in vitro study. Endodontology, 36(2), 120-124.