Enhancing Biological Response and Bone-Implant Contact through Surface Treatment of Dental Implants: Exploring Contemporary Techniques

Abstract:
Background:
Surface modification of dental implants plays a critical role in optimizing osseointegration and long-term clinical success. Conventional approaches such as sandblasting, acid etching, anodization, and plasma spraying have been widely explored, yet newer material science innovations continue to reshape implant surface engineering.

Objective:
This narrative review, evaluated using the Scale for the Assessment of Narrative Review Articles (SANRA), investigates contemporary surface treatment techniques and their influence on biological performance, bone–implant contact, and antibacterial efficiency.

Methods:
A comprehensive literature review of studies published between 2014 and 2024 was conducted to assess bioactive, nanostructured, and biochemical surface modifications. Eligible narrative reviews were critically appraised using SANRA to determine methodological rigor and transparency across included evidence.

Results:
Findings indicate that traditional coatings like hydroxyapatite and silica-based films enhance bioactivity, whereas nanostructured and biofunctionalized surfaces provide superior cellular responses and antimicrobial potential. SANRA-based scoring demonstrated a predominance of high- and medium-quality reviews, supporting the reliability of current findings.

Conclusion:
Recent advances in dental implant surface modifications underscore the value of integrating nanotechnology and biochemical strategies to improve biological outcomes. Emerging approaches such as ultraviolet photo functionalization, which restores titanium surface energy, and carbon nanomaterial-based coatings, which combine biocompatibility with enhanced mechanical resilience, represent promising directions for future clinical translation.

Keywords: Dental Implants, Surface Treatment, Bone-Implant Contact, Osseointegration, SANRA, Narrative Review

INTRODUCTION

Modern implant dentistry entails restoring and rehabilitating the complete oral environment and masticatory elements along with enhancing the compromised esthetics of an average patient.

Despite their widespread use, implant failures remain a coherent concern, often attributed to myriad factors, with unsatisfactory osseointegration being the primary cause.1 Although implant rehabilitation is generally successful, factors like the implant site, bone quality and quantity, and operator's experience can significantly affect treatment outcomes. The biomechanics of the bone-implant surfaces are significant to the stability and success of implants. The mechanical integrity of bone and associated implant surface directly influence the long-term stability of the bone-implant interface [1].

The variety of factors that affect the interface are: (i) surface roughness, (ii) partial bone-implant contact, (iii) adhesion of bone, (iv) time elapsed in the development of bone-implant adhesion. This complexity can be approached from multiple perspectives, such as examining bone–implant distance, mechanical behavior, and the dynamic aspect, which considers the remodeling of bonetissue around the implant over time [1,2].

As discovered by Branemark, the implant osseointegration phenomenon consists of the time evolution of bone in close approximation to implant thereafter to obtain a physio-mechanical connection between the implant and associated bone. To assess the efficiency of osseointegration, it is obligatory to measure the biomechanical properties of surrounding bone which has a complex nature to anisotropic, viscoelastic, and heterogenous properties [3]. Bone tissue also adapts its structure through remodeling to mechanical stresses.4 Regeneration of bone under implants takes a long duration as the temporal evolution and spatial distribution of the different properties of bone are heterogeneous. The protagonist osteoblast cell regeneration is dependent on (I) deposition of extracellular matrix, (II) production of hormones for mineralization with Ca and PO4 ions, (III) formation of woven bone, and (IV) remodeling to form mature bone. This process of formation of mature bone is affected by chemical pathway stresses. It is also a well-known fact that osteoclastic activity diminishes primary stability which in turn prevents implant micromotion. In age-old implant prosthodontics, it has been seen that implant surfaces have evolved to use micro-rough grade IV Cp-Ti or grade IV Ti alloys. “However, further research on modifications of implant surfaces requires micro-level, and nano-level research on understanding the feedback system of osseointegration. At the level of microtopography, surface modifications were focused on quantification of bone apposition. However, these modifications also resulted in the alteration of cellular behaviour in-vitro and bone physiology. Now, osseointegration is considered a phase in bone healing seen as if in an inflammatory response and modifications in its nano-topography, surface characteristics, and chemical changes to further enhance the response to benefit the healing process” [4,5]. Recently, surface modifications for the newer implant systems have been researched and thoroughly studied. Major modifications have been put forth by researchers globally. The most recent modifications can be seen well documented in narrative reviews spanning a decade. However, surface modifications have been repeated and some reviews lack accurate ad junctures. Therefore, for the purpose of this review of the recent literature focusing on the surface modifications discussed in them. We have used the SANRA tool for quality assessment. SANRA is a scale for the quality assessment of narrative review articles. It is a feasible, reliable and consistent scale for assessing narrative reviews based on their objectives and outcomes [6].

Clinical implications of the review—For this review, we have considered comprehensive (narrative) reviews by multiple authors from different countries. We aimed to find the most suitable and feasible implant surface modification in current prosthetic dentistry.

SEARCH STRATEGY

An electronic search was carried out on databases such as PubMed/ Medline, Scopus, Ebsco, Google Scholar, and Web of Science from 2014 up to 2024 using keywords, ‘biological surface treatment’, ‘surface coating’, ‘engineering principles in dental implants’, and ‘Nano topography’. First stage of the review included two independent authors SN and UB who searched various databases for titles as well as abstracts for relevant literature. Full-text reviews were screened by (SN, NJ and UB) three authors. Any disagreements that arose were resolved by consensus and by discussion with (PD)fourth reviewer. Third stage involved qualitative analysis of selected narrative reviews with SANRA tool.

Inclusion and exclusion criteria-

Articles published between 2014 till 2024 in the English language were included. Only narrative reviews were considered for the purpose of this article. Articles that discussed the use of multiple surface modifications on implants were preferred.

Articles published before 2014 were excluded. Systematic reviews and meta-analysis were not included and articles not using English language were not included.

Data acquisition-

The included narrative reviews were sorted by SN and UB. The data was entered in tabular form and checked for trueness by another author (PD). The table includes information about the author, year of publication, title of the review, outcomes studied and their conclusion.

Table 1- Included studies

| author/ year | title | country | outcomes | conclusion |
| --- | --- | --- | --- | --- |
| - F. Kunrath 2024 | Implant surface modifications and their impact on osseointegration and peri- implant diseases through epigenetic changes: A scoping revie | Sweden | The interplay among altered surface structures, varying chemical surface energies, and/or molecule release in oral tissues has been demonstrated to affect epigenetic processes in adjacent tissues due to a physical-chemical interaction. Epigenetic alterations concerning dental implants vary between health and disease states | . In conclusion, emerging approaches in surface modifications for dental implants functionalized with epigenetics have great potential with a significant impact on modulating bone healing during osseointegration |
| - Schinemann, 2019 | Histological evaluation of titanium fiber mesh-coated implants in a rabbit femoral condyle model | Belgium | Newly formed bone into mesh porosity was observed for all three types of im plants. Histomorphometric analyses revealed significantly higher (~2.5 fold) BA% values for TFM-22 implants (30.9 ± 9.5%) compared to Control implants | Finally, TFM-22 implants showed more and thicker trabeculae in the peri-implant region. |
| - Saran, 2023 | Advances in implant surface modifications to improve osseointegratio | Plasma spraying technology (PST), Plasma immersion ion implantation (PIII)., Laser cladding. Sandblasting and acid etching (SLA). | we systematically present the latest advances in surface modification techniques for orthopaedic implants, including mechanical, physical, chemical, and biological modification |  |
| - Edgahi M.A.etal jan 2022 | A practical review over surface modification, nanopatterns,emerging materials , drug delivery systems,and their biophysiochemical prperties for dental implants:recent progress and advances | Tehran,Iran | the article found that there is no gold standard for modifying an implant because the success rate depends on many parameters such as patients` general condition. | dominating and fabrication process is the key factor fpr producing the optimum geometries to aid in osteogenic function as well as engineered delivery system |
| - Yeo I.S. 2022 | Dental Implants Enhancing biological response through surface modifications | Seoul,Korea | There is weak bindings between SLA with calcium phosphate coatings .proteins usually exert vrious effects on a living system | implant surface treatment at nano level was consider ineffective for osteogenesis due to dimensional aspects of an osteon and incomplete bone ingrowth |
| - Walter N et.al may 2022 | Evolution of implants and advancements for osseointegration :A narrative review | Germany | Next to metal or inorganic compounds as coating materials, a variety of biomolecules (peptides) BMP growth factors, Non BMP growth factors, Collagens, Hyaluronic acid etc. is currently studied for their osteosupportive capacities | osseointegration can be improved by surface modification on the micro and nano scale |  |
| - Jambulkar N. | Surface modification techniques for different materials used in dental implants review | Nagpur,India | more research is needed to determine most effective porous implant design | titanium and zirconium materials are good for implant fabrication whereas SLA techniques provide better osseointegration |  |
| - Saghiri M.A. e.al 2021 | Current technology for identifying dental implants: a narrative review | U.S.A. | The development of a new and extensive database for implants is vital for the evergreen global increase in patients and treatment outcomes. | More research is needed to cover the market variety and the update for database is mandatory and essential for dental implant global production |  |
| - Rahimi S.N. et.al july 2021 | Surface modification of dental implant and its clinical performance: a review | Malaysia | Based on existing clinical data, minimally rough surface implants (0.5 to 1 micron) and rough surface implants (>2 micron) exhibit a low long-term survival rate of under 90%, while the majority of commonly used dental implants have a moderately rough surface | implant surface modification have also resulted in the change of surgical protocol from two stage to one stage surgery |  |
| - Shamaa A , arvina R 2021 | surface modification of dental implants- a review | India | current development in surface engineering techniques aims at gaining information in the properties,behaviour and the reaction of various materials | this article reviews the surface modification of dental impalnts for the achievements of better success rates |  |
| - Dong H et.al oct,2020 | Surface modification techniques and emerging functional coating of dental implants | China | Improvements in physical and chemical modification techniques have enhanced dental implant surfaces to speed up osseointegration, with the goal of reducing the edentulous duration for patients | this review comprehensively investigates and summarizes the modifying or coating methods of implant surfaces and analyzes the osteointegration and antibacterial characteristics of emerging functional coatings |  |
| - Kurup A et.al june,2020 | Surface modification techniques of titanium and titanium alloys for biomedical dental applications: a review | India | mechanical methods(acid ethching,grit blasting , hygrogen peroxide treatment,organic and inorganic coatings)have been experimentally proven to enhance the osseointegration rate. | the surface modification of the titanium implant surface significantly improves the properties of the implant |  |
| - Zafar M.S. et.al june,2020 | customized therapeutic surface coatings for dental implants | Pakistan | a range of surface modifications and coatings(antimicrobial ,bioactive,therapeutic drugs)have been explored for dental implants. | the present article reviews various interdisciplinary aspects of surface coatings on dental implants and its related therapeutic effects |  |
| - H. Chouirfa et al. dec 2019 | Review of titanium surface modification techniques and coatings for antibacterial applicatins | France | This review discusses various strategies to prevent infection on titanium surfaces: surface modifications and coatings using antibiotics, antimicrobial peptides, inorganic antibacterial metal elements, and antibacterial polymers | The increasingly popular research topic of active surfaces has permitted the flourishing development of new molecules that have not yet reached maturity. Improvements in scalability, animal and clinical testing are to be expected In the coming years before any standard arises. |  |
| - Hou C et.al march,2022 | Surface Modification Techniques to Produce Micro/Nano-scale Topographies on Ti-Based Implant Surfaces for Improved Osseointegration | China | This article examines the features and use of various titanium processing techniques, and investigates how different technologies influence surface traits, mechanical properties, cellular behavior, and osseointegration | The characteristics of the ideal surface-modified orthopedic implants in the future: mechanical properties close to that of bone, ability to promote bone healing, antibacterial ability, sufficient service life, easy to remove without complications, individualization, and highly automated and environmentally friendly treating process. |  |
| - Kligman S et.al april 2021 | The Impact of Dental Implant Surface Modifications on Osseointegration and Biofilm Formation | U.S.A. | Optimal modifications improve the connection between the implant's surface and the adjacent bone, promoting osseointegration and reducing bacterial colonization to lower the chance of biofilm development | However, all the tested implants in these studies are regular titanium implants. Investigating a proper combination of implant site osteotomy, implant material, and implant surface modification strategy has the great potential to improve the implant success rate, especially for the patients who have poor bone quality in the implant sites |  |
| - Chang L.C. sep,2022 | Clinical Applications of Photofunctionalization on Dental Implant Surfaces: A Narrative Review | Taiwan | Photofunctionalization can also enhance cellular migration, attachment, and proliferation, thereby promoting osseointegration and coronal soft tissue seal. | However, PhF did not overcome the dental implant challenge of oral cancer cases. It is necessary to have more clinical trials focused on complex implant cases and non-dental fields in the future. |  |
| - Khaohoen A et.al nov,2023 | Biomaterials and Clinical Application of Dental Implants in Relation to Bone Density—A Narrative Review | Thailand | In low-density scenarios, it's advisable to use a conical titanium implant design with greater length, wider diameter, inverse buttress features, self-tapping capability, finer thread pitch, and deeper thread depth | Implant material, implant design, surgical techniques, and bone density are pivotal factors affecting the success rates of dental implant placement in low-density bone. Further study is required to find the optimal implant material for a clinical setting's bone state. |  |
| - Inchingolo A.M. may ,2023 | Surface Coatings of Dental Implants: A Review | Italy | An examination of various implant surface coatings was conducted to determine optimal surfaces that enhance osseointegration, epithelial adherence to the implant area, and general peri-implant health | Implant surfaces must have antibacterial capabilities to prevent peri-implant disease. Research still needs to improve implant material to minimize clinical failure. |  |
| - Yeo S.L. dec,2019 | Modifications of Dental Implant Surfaces at the Micro-and Nano-Level for Enhanced Osseointegration | Korea | Recent research findings indicate that osteogenic cells react to nanoscale chemical and morphological alterations on surfaces, such as titanium dioxide nanotube configurations, functional peptide coatings, fluoride treatments, calcium-phosphorus applications, and ultraviolet photofunctionalization | Some of the nano-level modifications have not yet been clinically evaluated. However, these modified dental implant surfaces at the nanoscale have shown excellent in vitro and in vivo results, and thus promising potential future clinical use. |  |
| - Haugen H.J. et.al july,2022 | The Antibacterial and Cytotoxic Effects of Silver Nanoparticles Coated Titanium Implants: A Narrative Review | Norway | The analyzed research indicated that silver nanoparticles on dental implant surfaces decreased cytotoxicity while offering a lasting antibacterial effect. The cytotoxic and antibacterial properties are closely related to the release rate of silver nanoparticles from titanium surfaces, with a slower release enhancing cell viability and proliferation | to improve the clinical translation, there is still a need for more studies, especially evaluating the long-term systemic effects and studies recreating the conditions in the oral cavity. |  |
| - Bokobza L june,2024 | On the Use of Nanoparticles in Dental Implants | France | Carbon nanomaterials such as carbon nanotubes, graphene, and its derivatives (including graphene oxide and graphene quantum dots) can function as coatings for the surface of implants. Their antibacterial characteristics and potential for being modified with suitable chemical groups render them especially effective in enhancing biocompatibility and facilitating osseointegration | Another interesting approach, already applied in polymer nanocomposites, is the use of mixtures of nanoparticles of different morphologies that may exhibit better properties than each single type of particles on account of possible synergistic effects. This will allow for a decrease in the amount of nanomaterial with potential toxicity. |  |
| - Ciszynski M aug,2024 | Zirconia Dental Implant Designs and Surface Modifications:A Narrative Review | Germany | Zirconia's biocompatibility and ability to osseointegrate appears unquestionably good. Despite some of its mechanical properties being, factually, inferior to those of titanium, the benefits seem to outweigh the drawbacks | Zirconia implants show very good success rates in clinical research. This is partially due to available methods of surface treatment, including nanotopography alterations, which allow for improved wettability, bone-to-implant contact, and osteointegration in general. |  |
| - Tilikampee S april,2024 | Titanium Surface Modification Techniques to Enhance Osteoblasts and Bone Formation for Dental Implants: A Narrative Review on Current Advances | Thailand | This review highlights the effectiveness of various subtraction and addition methods in improving the surface characteristics of titanium dental implants, fostering positive results regarding osteoblast activity and bone development to varying extents | further investigation of factors playing a role in the dynamic osseointegration process in addition to osteoblasts and their functions, as well as improved surface modification techniques for the treatment of compromised patients, is greatly required. |  |
| - Marasli C june,2024 | Nano-Based Approaches in Surface Modifications of Dental Implants: A Literature Review | Greece | Peri-implantitis prevention can be achieved through the inherent antibacterial properties of metal nanoparticles and chitosan or hybrid coatings bearing antibiotic substances. | even though these modifications have shown promising results, future research is necessary to assess their clinical behavior in humans and proceed to widespread commercialization |  |

Cad-Cam coatings

Composition

Early dental implants, dating back to the 16th and 17th centuries, were made of stone and ivory, followed by metal implants made of iridium, tantalum, gold, lead, and stainless steel in the late 20th century. Historically, metals, ceramics, and polymers have been favored materials. Hydroxyapatite (HA), a ceramic known for its biocompatibility and ability to promote bone regeneration, has been used as a surface coating due to its low mechanical strength. Hahn and Vassos reported a 97.8% success rate, though degradation of the ceramic coating was noted. Today, commercially pure titanium (Cp Ti) is the preferred material, with studies by Karl et al. showing a survival rate of over 99% after one year and 95% after ten years for Ti-Unite surface implants. However, titanium's low Young’s modulus makes it overly stiff, leading to the development of micro milling techniques to enhance the biomechanical response. Recent research on zirconium implants has shown poor bone-to-implant adhesion, with most studies being short-term and lacking long-term clinical evidence [7].

Surface treatments and modification

1. IMPLANT SURFACE DESIGN AND BIO MODIFICATIONS

Surface morphology and coating is critical aspect when designing and manufacturing an implant. The implants survival parameters largely depend on engineering strategies such as sandblasting, plasma spraying, anodization, laser ablation, and acid-etching [8].

  - Sandblasting

This process involves projection of accelerated microspheres of TiO2, Al2O3, SiO2 and Hydroxyapatite. Gonshor A, et al [9] in an observational long-term study demonstrated a higher overall clinical outcome for the sandblasted implants. The factors that are critical in achieving a successful sandblasted implants are distance from projection gun to implant surface, the pressure applied by the gun, saturation time and projection diameter.

  - Acid-Etching:

In this process, strong acids are used to remove the oxide layer from the titanium implant surface along with some part of the underlying material that results in homogenous surface roughening (0.5 to 2μm), increased surface area, and enhanced bio adhesion. A concentrated solution of HNO3 and HF or a mixture of HCl and H2SO4 is frequently used [10] Osseotite (Zimmer Biomet, Warsaw, IN, USA) is an example of a commercial implant manufactured using this technique. In a study conducted by Giner, et al [11] in 2018, superior bone-implant contact was seen 3-6 weeks after implant insertion. The removal torque values were also 4 times higher than the machined surfaces. This procedure is carried out in conjunction with sandblasting wherein; acid etching erosion is carried out after sandblasting the implant surface. This leads to an augmentation of surface roughness (sandblasting) and micro-texture and clean up with acid-etching culminating into the osteoblastic invasion. Higher success and persistence rates were found by Cochran et al after 5 years when these implants were loaded [12]. TiO2 grit-blasted implants reported a success rate of 96.9% by Rasmusson, et al [13], and these implants had a higher success rate than unblasted, machine-turned implants.

  - Anodization:

The core process in this technology involves the change in the distinctive oxide layer that makes it more biocompatible and mononuclear cells were seen adhering to the implant surface. The process involves voltage application on a titanium implant immersed in an electrolyte solution resulting in production of micropores (contrasting diameter) [14].  TiUnite (Nobel Biocare, Gothenberg, Sweden) surface altered by this technique showed that only 8.2% implants were affected by peri-implantitis as there was an improvement in osseointegration in a study conducted by Degidi M, et al [15] in 2012.

  - Hydroxyapatite Coating Surface:

The hydroxyapatite (Ca10 (PO4)6(OH)2 coating at the implant surface is considered bioactive as it results in the formation of a layer of calcium phosphate on the implant surface through solid solution ion exchange. This layer is developed via octacalcium phosphate (equivalent to hydroxyapatite) that is incorporated in the developing bone [16] Several methods employed to achieve hydroxyapatite coatings are plasma-spraying, electrochemical deposition, high-velocity suspension plasma-spraying and sol-gel dip coating method [17].

2. Biomimetic Organic and Inorganic Coatings:

Biomimetic dental implants are considered as one of the recent clinical developments in implant surface modification. Different surface coatings and surface changes have been studied in order to improve osseointegration and heal the peri-implant tissues. These coatings are divided into organic and inorganic depending on their structure. They have varying thicknesses and roughness that may affect the overall dental implant surface’s chemical, physical, biological and mechanical properties.

3. Antifouling Coatings:

The coatings that have been employed for this are hydrophilic polymers, zwitterionic materials, and superhydrophobic materials. Hydrophilic polymer, for eg: PEG (polyethylene glycol), acts against protein adsorption through a stearic-repulsion mechanism. A layer is formed around this through the structured barrier which acts as a physical hindrance for protein and pathogens. Long-polymer chains are more efficient than self-assembled monolayers (SAM) PEG coatings. SAMs for dental implantology have recently gained popularity as a simple and accurate method of customising surface characteristics due to their ability to adjust the chemical properties of the interface at the molecular level. This is because these systems are composed of well-organised organic components.

The major disadvantage of this coating is the rapid auto-oxidation when exposed to oxygen that can affect the long-term durability [18]. Another antifouling agent zwitterionic 2-methacryloyloxyethyl phosphorylcholine (MPC) reduces the retention of Candida albicans, Staphylococcus aureus, Pseudomonas aeruginosa, Streptococcus mutans and retention of peri-implant pathogens. The above is attributed to the superhydrophilicity of this coating. In some cases, they are also combined with quarternary ammonium compounds (QAC) to have a synergistic effect [19]. Super hydrophilic materials (contact angle greater than 150 ̊) demonstrate less wettability and reduce the adhesion of molecules and cells on the implant surface. Souza JGS, et al [20] 's research led to the development of a one-step method for fabricating this coating using glow discharge plasma.

RESULTS

Included reviews

We had identified 25 narrative reviews which were eligible for our investigation. The SANRA questionnaire was used to appraise these narrative reviews by 3 reviewers (SN, NJ and UB) and scores were given individually to each article after discussion and consensus was reached. The score card for the included reviews is depicted as below

Table 2- SANRA Score Card

| Author and Year | Question 1 | Question 2 | Question 3 | Question 4 | Question 5 | Question 6 | Total score |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Schunemann F et al, 2019 | 1 | 1 | 0 | 2 | 1 | 2 | 7 |
| Chouirfa H et al, 2019 | 2 | 2 | 2 | 2 | 1 | 2 | 10 |
| Yeo S.L et al, 2019 | 0 | 1 | 0 | 2 | 1 | 2 | 6 |
| Dong H et al, 2020 | 2 | 1 | 0 | 2 | 2 | 2 | 9 |
| Kurup A et al, 2020 | 2 | 1 | 0 | 2 | 1 | 2 | 8 |
| Zafar M.S et al,2020 | 1 | 1 | 2 | 2 | 1 | 2 | 9 |
| Saghiri M.A et al, 2021 | 2 | 1 | 2 | 2 | 1 | 1 | 9 |
| Rahimi S.N et al, 2021 | 2 | 2 | 1 | 1 | 1 | 2 | 9 |
| Shamaa A et al, 2021 | 1 | 0 | 0 | 1 | 1 | 0 | 3 |
| Kligman S et al, 2021 | 2 | 2 | 2 | 2 | 2 | 2 | 11 |
| Edgahi M.A et al, 2022 | 1 | 2 | 1 | 1 | 1 | 2 | 8 |
| Hou C et al, 2022 | 2 | 2 | 0 | 2 | 1 | 2 | 9 |
| Jambulkar N, 2022 | 1 | 1 | 1 | 2 | 1 | 2 | 8 |
| Walter N et al, 2022 | 1 | 2 | 0 | 1 | 1 | 1 | 6 |
| Yeo I et al, 2022 | 2 | 1 | 0 | 1 | 1 | 1 | 7 |
| Chang L et al, 2022 | 1 | 0 | 0 | 2 | 1 | 0 | 6 |
| Haogen H et al, 2022 | 1 | 0 | 1 | 2 | 1 | 2 | 6 |
| Khaohoen A et al, 2023 | 1 | 1 | 1 | 2 | 2 | 1 | 9 |
| Inchigolo A et al, 2023 | 1 | 2 | 2 | 2 | 1 | 1 | 10 |
| Saran R, 2023 | 1 | 2 | 2 | 1 | 1 | 2 | 9 |
| Kurnath M et al, 2024 | 1 | 1 | 2 | 1 | 2 | 2 | 9 |
| Bokoza L et al, 2024 | 0 | 0 | 1 | 1 | 0 | 0 | 2 |
| Tilikampee S et al, 2024 | 1 | 2 | 2 | 2 | 2 | 1 | 9 |
| Marasli C et al, 2024 | 1 | 0 | 1 | 2 | 2 | 1 | 7 |
| Ciszynski M, 2024 | 1 | 1 | 0 | 0 | 1 | 1 | 4 |

Among the 25 narrative review articles appraised using the SANRA tool, total scores ranged from 2 to 11, with a mean score of 7.68±2.167.68±2.16. Out of the included studies, 12 reviews (48%) were rated as high quality (score ≥9), 10 (40%) as medium quality (score 6–8), and 3 (12%) as low quality (score <6). The majority of reviews demonstrated satisfactory scientific rigor, especially in literature search reporting and clear referencing, while common weaknesses included inconsistent articulation of aims and inadequate data presentation in lower-scoring reviews. These findings support an overall moderate to high level of methodological quality among recent narrative reviews of dental implant surface modifications.

Table 3- Statistical Data

| Parameter | Value / Description |
| --- | --- |
| Total number of reviews analyzed | 25 |
| Individual SANRA Scores (out of 12) | 7, 10, 6, 9, 8, 9, 9, 9, 3, 11, 8, 9, 8, 6, 7, 6, 6, 9, 10, 9, 9, 2, 9, 7, 4 |
| Mean ± SD | 7.68 ± 2.16 |
| Range | Minimum = 2, Maximum = 11 |
| High Quality (≥9) | 12 reviews (48%) |
| Medium Quality (6–8) | 10 reviews (40%) |
| Low Quality (<6) | 3 reviews (12%) |

Fig 1:

DISCUSSION

Recent advancements in dental biomaterial surface modifications have focused on enhancing osseointegration, antibacterial properties, and overall implant performance. According to the quality assessment, we have found 12 high quality, 10 medium quality and 3 low quality narrative reviews. The narrative reviews which have been denoted “high quality”. Each section pertaining to the scores are discussed below-

The high score index articles

Inchingolo et al. (2023) [21] identified the role of surface coatings in improving osseointegration, epithelial attachment, and peri-implant health, stressing the need for antibacterial surfaces and material advancements to prevent clinical failures. Kligman et al. (2021) [22] emphasized balancing osseointegration enhancement with biofilm reduction, particularly for patients with poor bone quality. Chouirfa et al. (2019) [23] examined methods for preventing infections on titanium surfaces, emphasising surface coatings and alterations that use polymers, antibiotics, antimicrobial peptides, and antibacterial metals. While promising, these approaches require improvements in scalability, as well as extensive animal and clinical testing, before standardized solutions emerge. Saghiri et al. (2021) [24] highlighted the need for a comprehensive global dental implant database to address increasing patient demands.

Techniques like laser texturing, highlighted by Saran et al. (2023) [25], provide superior surface alterations compared to traditional methods by creating innovative patterns without compromising bulk properties. Nano-topographical changes, as explored by Yeo (2022) [26], influence early bone response and hydrophilicity, although their clinical application remains under investigation. Dong et al. (2020) [27] summarized advancements in physical and chemical surface modification techniques, emphasizing their role in enhancing osseointegration and reducing the edentulous period through functional coatings. Similarly, Zafar et al. (2020) [28] explored a range of therapeutic surface modifications and coatings, including antimicrobial, bioactive, and drug-loaded coatings, underscoring their interdisciplinary therapeutic potential for dental implants. Rahimi et al. (2021) [29] noted that moderately rough surfaces dominate commercially due to higher survival rates, while surface modifications have enabled a shift to one-stage surgery. Similarly, photo functionalization, as described by Chang (2022) [30], improves surface wettability, removes aging-related hydrocarbon contaminants, and promotes cell migration and proliferation, thereby optimizing osseointegration.

Medium score index articles

Yeo I.S. (2022) [31] highlighted weak bonds between SLA surfaces and calcium phosphate coatings, suggesting nano-level treatments are ineffective for osteogenesis due to incomplete bone ingrowth. Kurup et al. (2020) [32] demonstrated that mechanical methods, such as acid etching and grit blasting, enhance osseointegration and implant properties. Edgahi et al. (2022) [33] emphasized that no gold standard exists for surface modification, as success depends on multiple parameters, including patient conditions and fabrication processes. Jambulkar (2020) [34] pointed to titanium and zirconium as favourable materials and SLA as superior for osseointegration, calling for further research on porous implant designs. Walter et al. (2022) [35] reviewed the osteosupportive potential of biomolecules like peptides and growth factors, stressing micro- and nanoscale surface modifications for improved osseointegration. Yeo S.L. (2019) [36] showed nanoscale modifications, including peptide coatings and UV photo functionalization, deliver promising in vitro and in vivo results, though further clinical validation is needed. Haugen et al. (2022) [37] found silver nanoparticle-coated implants provide prolonged antibacterial effects with minimal cytotoxicity but require more studies on long-term systemic effects and oral cavity conditions. Chang L.C. (2022) [38] reported that photo functionalization enhances osseointegration and tissue sealing but remains insufficient for complex cases like oral cancer, necessitating further clinical trials.

Low score index articles

Anjum et al (2021) [39] reviewed advancements in surface engineering techniques aimed at enhancing the understanding of material properties, behaviour, and reactions to improve dental implant success rates. However, the study lacks detailed discussion on specific coating materials, nanoscale modifications, and clinical applications explored in previous studies. Bokobza (2024) [40] highlighted the potential of carbon nanomaterials, such as graphene and its derivatives, for dental implant coatings due to their antibacterial properties, biocompatibility, and functionalization potential. The study also proposed combining nanoparticles of different morphologies to achieve synergistic effects while minimizing toxicity. Nevertheless, as noted in earlier reviews, the study lacks long-term clinical evaluations and practical comparisons with conventional coating methods. Ciszynski (2024) [41] emphasized zirconia implants' favourable biocompatibility, osseointegration potential, and success rates, facilitated by surface treatments like nano topography modifications that improve wettability and bone-to-implant contact. While zirconia's mechanical properties are considered inferior to titanium, the study does not address antibacterial strategies or nanoscale advancements seen in previous studies, leaving room for further exploration of hybrid approaches and long-term performance. Nanomaterials play a pivotal role in modern implantology. Marasli et al. (2024) [42] emphasized the antibacterial benefits of coatings with metal nanoparticles and chitosan, which prevent peri-implantitis. Similarly, Edgahi et al. (2022) [33] reviewed the synergistic effects of nanopatterns and antibacterial nanoparticles, suggesting their role in reducing microbial infection while promoting osteogenesis. Despite these advancements, as Haugen et al. (2022) [37] noted, long-term studies are needed to evaluate the systemic effects of such modifications.

Titanium remains the gold standard for dental implants, with surface modifications continuing to evolve. Techniques like sandblasting, acid-etching, and anodic oxidation, reviewed by Yeo et al. (2020) [31], have consistently shown high survival rates. Tuikampee et al. (2024) [43] and Jambhulkar et al. (2022) [34] highlighted the effectiveness of these methods in enhancing osteoblast activity and bone formation. Emerging strategies, such as epigenetic modifications (Kunrath et al., 2024) [44], offer exciting prospects for improving bone healing during osseointegration. Future narrative reviews should aim to provide a more comprehensive synthesis by including systematic comparisons of various implant surface modification techniques and evaluating their efficacy, long-term performance, and clinical outcomes. Key recommendations for future research should include comparative analysis, clinical trials, synergistic approaches, toxicity and biocompatibility, standardization, and scalability of materials.

CONCLUSION

Advancements in dental implant surface modifications have significantly improved implant performance by enhancing osseointegration, antibacterial properties, and hard tissue response. From laser texturing and nano-topographical modifications to the incorporation of nanomaterials and drug delivery systems, these innovations demonstrate immense potential to optimize implant success. Titanium remains the material of choice, with well-established techniques like sandblasting and acid-etching consistently delivering favorable outcomes. Emerging strategies, such as photo functionalization, epigenetic modifications, and carbon-based nanomaterials, offer promising avenues for further improving implant efficacy and longevity. However, despite these developments, the need for comprehensive, long-term clinical trials persists to validate these techniques, standardize protocols, and ensure their safe and effective application in diverse clinical scenarios. By addressing these gaps, future research can help translate these advances into routine clinical practice, ultimately enhancing patient outcomes in implant dentistry.

CONFLICT OF INTEREST

There was no conflict of interest.

Disclaimer (Artificial intelligence)

Author(s) hereby declare that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc.) and text-to-image generators have been used during the writing or editing of this manuscript.

REFERENCES

- Debbarma L. Restoring oral health: implant-supported full-mouth rehabilitation for an edentulous patient. Cureus. 2024 Aug 12;16(8):e66732. doi: 10.7759/cureus.66732.

- Gao X, Fraulob M, Haïat G. Biomechanical behaviours of the bone-implant interface: a review. J R Soc Interface. 2019 Jul 26;16(156):20190259. doi: 10.1098/rsif.2019.0259.

- Cooper LF, Shirazi S. Osseointegration—the biological reality of successful dental implant therapy: a narrative review. Front Oral Maxillofac Med. 2022 Dec 30;4. doi: 10.21037/fomm-21-77.

- Brand RA. Biographical sketch: Julius Wolff, 1836-1902. Clin Orthop Relat Res. 2010 Apr;468(4):1047-9. doi: 10.1007/s11999-010-1258-z.

- Inchingolo AM, Malcangi G, Ferrante L, Del Vecchio G, Viapiano F, Inchingolo AD, et al. Surface coatings of dental implants: a review. J Funct Biomater. 2023 May 22;14(5):287. doi: 10.3390/jfb14050287.

- Baethge C, Goldbeck-Wood S, Mertens S. SANRA—a scale for the quality assessment of narrative review articles. Res Integr Peer Rev. 2019;4:5. doi: 10.1186/s41073-019-0064-8.

- Abraham CM. A brief historical perspective on dental implants, their surface coatings and treatments. Open Dent J. 2014 May 16;8:50-5. doi: 10.2174/1874210601408010050.

- Accioni F, Vázquez J, Merinero M, Begines B, Alcudia A. Latest trends in surface modification for dental implantology: innovative developments and analytical applications. Pharmaceutics. 2022 Feb 21;14(2):455. doi: 10.3390/pharmaceutics14020455.

- Gonshor A, Goveia G, Sotirakis E. A prospective, multicenter, 4-year study of the ACE Surgical Resorbable Blast Media implant. J Oral Implantol. 2003;29(3):174-80. doi: 10.1563/1548-1336(2003)029<0174:APMSOT>2.3.CO;2.

- Kligman S, Ren Z, Chung CH, Perillo MA, Chang YC, Koo H, et al. The impact of dental implant surface modifications on osseointegration and biofilm formation. J Clin Med. 2021 Apr 12;10(8):1641. doi: 10.3390/jcm10081641.

- Giner L, Mercade M, Torrent S, Punset M. Double acid etching treatment of dental implants for enhanced biological properties. J Appl Biomater Funct Mater. 2018 Apr;16(2):83-9. doi: 10.5301/jabfm.5000376.

- Cochran DL, Buser D, Ten Bruggenkate CM. The use of reduced healing times on ITI implants with a sandblasted and acid-etched (SLA) surface: early results from clinical trials on ITI and SLA implants. Clin Oral Implants Res. 2002;13(2):144-53. doi: 10.1034/j.1600-0501.2002.130204.x.

- Rasmusson L, Roos J, Bystedt H. A 10-year follow-up study of titanium dioxide-blasted implants. Clin Implant Dent Relat Res. 2005;7(1):36-42. doi: 10.1111/j.1708-8208.2005.tb00045.x.

- Mishra SK, Kumar MA, Chowdhary R. Anodized dental implant surface. Indian J Dent Res. 2017 Jan-Feb;28(1):76-99. doi: 10.4103/ijdr.IJDR_386_16.

- Degidi M, Nardi D, Piattelli A. 10-year follow-up of immediately loaded implants with TiUnite porous anodized surface: 10-year follow-up of TiUnite surface. Clin Implant Dent Relat Res. 2012 Sep;14(5):828-38. doi: 10.1111/j.1708-8208.2012.00446.x.

- Łukaszewska-Kuska M, Krawczyk P, Martyla A, Hędzelek W, Dorocka-Bobkowska B. Hydroxyapatite coating on titanium endosseous implants for improved osseointegration: physical and chemical considerations. Adv Clin Exp Med. 2018 Aug;27(8):1055-9. doi: 10.17219/acem/69084.

- Sharma A. Hydroxyapatite coating techniques for titanium dental implants—an overview. Qeios [Internet]. 2023 [cited 2025 Oct 16];1-14. Available from: doi.org/10.32388/2E6UHN

- Buxadera-Palomero J, Canal C, Torrent-Camarero S, Garrido B, Gil FJ, Rodríguez D. Antifouling coatings for dental implants: polyethylene glycol-like coatings on titanium by plasma polymerization. Biointerphases. 2015;10(2):029505. doi: 10.1116/1.4913376.

- Ramburrun P, Pringle NA, Dube A, Adam RZ, D’Souza S, Aucamp M. Recent advances in the development of antimicrobial and antifouling biocompatible materials for dental applications. Materials (Basel). 2021 Jun 9;14(12):3167. doi: 10.3390/ma14123167.

- Rao Q, Weng L, Zhang J, Liu D, Zhang W, Chen S, et al. Research progress in superhydrophobic titanium-based implants for antibacterial applications. Coatings. 2023;13(2):419. doi: 10.3390/ma14123167.

- Inchingolo AM, Malcangi G, Ferrante L, Del Vecchio G, Viapiano F, Inchingolo AD, et al. Surface coatings of dental implants: a review. J Funct Biomater. 2023 May 22;14(5):287. doi: 10.3390/jfb14050287.

- Kligman S, Ren Z, Chung CH, Perillo MA, Chang YC, Koo H, et al. The impact of dental implant surface modifications on osseointegration and biofilm formation. J Clin Med. 2021 Apr 12;10(8):1641. doi: 10.3390/jcm10081641.

- Chouirfa H, Bouloussa H, Migonney V, Falentin-Daudré C. Review of titanium surface modification techniques and coatings for antibacterial applications. Acta Biomater. 2019 Jan 1;83:37-54. doi: 10.1016/j.actbio.2018.10.036.

- Saghiri MA, Freag P, Fakhrzadeh A, et al. Current technology for identifying dental implants: a narrative review. Bull Natl Res Cent. 2021;45(1):7. doi: 10.1186/s42269-020-00471-0.

- Saran R, Ginjupalli K, George SD, Chidangil S, Unnikrishnan VK. LASER as a tool for surface modification of dental biomaterials: a review. Heliyon. 2023 Jun 1;9(6):e17457. doi: 10.1016/j.heliyon.2023.e17457.

- Dong H, Liu H, Zhou N, Li Q, Yang G, Chen L, et al. Surface modified techniques and emerging functional coating of dental implants. Coatings. 2020 Nov 10;10(11):1012. doi: 10.3390/coatings10111012.

- Zafar MS, Fareed MA, Riaz S, Latif M, Habib SR, Khurshid Z. Customized therapeutic surface coatings for dental implants. Coatings. 2020 Jun 17;10(6):568. doi: 10.3390/coatings10111012.

- Rahimi SN, Tengku Mohd Ariff TF, Kamar Affendi NH, Ahmad R. Surface modifications of dental implant and its clinical performance: a review. Compend Oral Sci (CORALS). 2022;9(1):52-66. doi: 10.24191/cos.v9i1.16907.

- Chang LC. Clinical applications of photofunctionalization on dental implant surfaces: a narrative review. J Clin Med. 2022 Sep 30;11(19):5823. doi: 10.3390/jcm11195823.

- Yeo IS. Dental implants: enhancing biological response through surface modifications. Dent Clin North Am. 2022 Oct;66(4):627-42. doi: 10.1016/j.cden.2022.05.009.

- Kurup A, Dhatrak P, Khasnis N. Surface modification techniques of titanium and titanium alloys for biomedical dental applications: a review. Mater Today Proc. 2021 Jan 1;39:84-90. doi: 10.1016/j.matpr.2020.06.163.

- Akbari Edgahi M, Naghib SM, Emamian A, Ramezanpour H, Haghiralsadat F, Tofighi D. A practical review over surface modification, nanopatterns, emerging materials, drug delivery systems, and their biophysiochemical properties for dental implants: recent progresses and advances. Nanotechnol Rev. 2022 Jan 27;11(1):637-79. doi: 10.1515/ntrev-2022-0037.

- Jambhulkar N, Jaju S, Raut A. Surface modification techniques for different materials used in dental implants review. Mater Today Proc. 2022 Jan 1;60:2266-9. doi: 10.1016/j.matpr.2022.04.683.

- Walter N, Stich T, Docheva D, Alt V, Rupp M. Evolution of implants and advancements for osseointegration: a narrative review. Injury. 2022 Nov;53 Suppl 2:S69-73. doi: 10.1016/j.injury.2022.05.057.

- Yeo IS. Modifications of dental implant surfaces at the micro- and nano-level for enhanced osseointegration. Materials (Basel). 2019 Dec 23;13(1):89. doi: 10.3390/ma13010089.

- Haugen HJ, Makhtari S, Ahmadi S, Hussain B. The antibacterial and cytotoxic effects of silver nanoparticles coated titanium implants: a narrative review. Materials (Basel). 2022 Jul 19;15(14):5025. doi: 10.3390/ma15145025.

- Chang LC. Clinical applications of photofunctionalization on dental implant surfaces: a narrative review. J Clin Med. 2022 Sep 30;11(19):5823. doi: 10.3390/jcm11195823.

- Anjum S, Shamaa B, Rajasekar A. Surface modification of dental implants—a review. J Evol Med Dent Sci. 2021 Apr 26;10(17):1246-51. doi: 10.14260/jemds/2021/265.

- Bokobza L. On the use of nanoparticles in dental implants. Materials (Basel). 2024 Jun 29;17(13):3191. doi: 10.3390/ma17133191.

- Ciszyński M, Chwaliszewski B, Simka W, Dominiak M, Gedrange T, Hadzik J. Zirconia dental implant designs and surface modifications: a narrative review. Materials (Basel). 2024 Aug 25;17(17):4202. doi: 10.3390/ma17174202.

- Marasli C, Katifelis H, Gazouli M, Lagopati N. Nano-based approaches in surface modifications of dental implants: a literature review. Molecules. 2024 Jun 27;29(13):3061. doi: 10.3390/molecules29133061.

- Tuikampee S, Chaijareenont P, Rungsiyakull P, Yavirach A. Titanium surface modification techniques to enhance osteoblasts and bone formation for dental implants: a narrative review on current advances. Metals. 2024 Apr 28;14(5):515. doi: 10.3390/met14050515.

- Kunrath MF, Garaicoa-Pazmino C, Giraldo-Osorno PM, Haj Mustafa A, Dahlin C, Larsson L, et al. Implant surface modifications and their impact on osseointegration and peri-implant diseases through epigenetic changes: a scoping review. J Periodontol Res. 2024 May 15. doi: 10.1111/jre.13273.