Parametric Dispersion and Amplification Characteristics in Magnetized Quantum Plasmas: A study about Spin Effect

.

ABSTRACT

In the present paper, the spin effect in parametric amplification and dispersion characteristics are determined by implementing the Quantum Magnetized Hydrodynamic (QMHD) model. The QMHD model is extended for spin dynamics and the spin effect is analytically investigated in a n-type piezoelectric semiconductor plasma. We have considered that the origin of the parametric amplification and dispersion relation lies in the second-order susceptibility arising from the nonlinear induced current density. The study shows that the parametric process is modified by including the quantum effect, especially the spin effect in the formulation. Furthermore, the results indicate that the spin effect can significantly alter the nonlinear optical response of materials, making it an important consideration in the design and optimization of nonlinear optical devices. The findings obtained from this study can be useful in designing and optimizing semiconductor devices for various quantum applications, such as sensors and actuators. Additionally, the study provides a deeper understanding of the fundamental quantum plasma physics behind the nonlinear optical response of materials.

Keywords: Quantum Plasma; Laser-plasma interaction; Parametric Interaction, parametric amplification

1. INTRODUCTION

Electron spin effects [1-5] have widened the emerging interest in plasma physics and opened new avenues for studying the behaviour of plasmas, particularly magnetic properties, and collective behaviour. The interest in spin also sparked research into novel applications such as spin-based plasma diagnostics and control techniques, which have the potential to revolutionize various fields including fusion energy, materials science, and quantum computing. Furthermore, the spin effect has also led to advancements in the field of spintronics, where the manipulation and control of electron spins are utilized for information storage and processing. This has paved the way for the development of more efficient and faster electronic devices, with potential applications in areas such as data storage and communication technology. Spin effects are crucial for developing advanced plasma-based technologies and improving our knowledge of astrophysical plasmas.

“The spin of electrons causes the spin-current interaction, i.e., the interaction of the magnetic moments and electric currents via the magnetic field. These interactions change the dispersion and absorption characteristics of plasma and develop a deeper understanding of how waves and instabilities spread out in the plasma medium. Ever since then, various phenomena have been studied for spin-1/2 quantum plasmas” [6-10]. These phenomena include spin waves, spin vortices, and spin-charge separation, which have all been observed in experiments and simulations. Understanding these phenomena is crucial for developing new technologies, which rely on the manipulation of electron spins in solid-state devices. Additionally, the study of spin has also led to advancements in the field of quantum magnetohydrodynamics, further enhancing our understanding of the complex behaviour of plasmas at the quantum level.

The QMHD model comprises a set of equations that show how charge, momentum, and energy move through systems of charged particles that interact through an electrostatic potential [11-12]. Mathematically, the QMHD model generalizes the fluid model for plasmas with the inclusion of quantum forces: i) quantum diffraction; ii) spin force with Fermi pressure. Quantum diffraction is considered Bohm's potential in electron motion under the influence of fields. The inclusion of quantum forces in the QMHD model allows for a more accurate representation of plasma behaviour, particularly at small scales where quantum effects become significant [13-15].

In the presence of an external magnetic field, the electron spins tend to align in the direction of the field. The variation of the magnetic field occurs on a timescale shorter than the characteristic spin-relaxation time. The degree of spin alignment can be approximated as a constant, which produces density fluctuations. The density fluctuation in the medium leads to the emergence of spin forces, which leads to our interest in studying the spin effect in piezoelectric semiconductor plasma dynamics.

“The spin forces play a crucial role in determining the overall behaviour of the plasma, as they contribute to the momentum transfer equations in the QMHD model” [16-18]. “The collective motion of quantum particles in magnetic fields gives a natural extension to the classical magnetohydrodynamic (MHD) theory in terms of the spin effect. Spin-1/2 quantum magnetohydrodynamic (QMHD) was recently proposed” [19-21] with the spin effect due to electrons by using Pauli equations of individual particles.

In this paper, we use analytical methods to investigate the spin effect in an n-type piezoelectric semiconductor plasma medium via parametric processes, and this approach allows us to investigate the impact of spin on the behaviour of quantum particles. We have considered that the origin of the dispersion and amplification characteristics lies in the second-order susceptibility arising from the nonlinear induced current density. The spin effect modifies the amplification characteristics by introducing an additional term in the governing equations, which accounts for the spin polarization of the particles. This modification leads to significant changes in the wave propagation and energy transport properties of the system. Additionally, our analysis reveals that the spin effect can also influence the stability and dynamics of quantum particles in this medium, opening new possibilities for controlling and manipulating their behaviour.

2. Theoretical formulation

The parametric characteristics of highly doped magnetized semiconductors, arising due to nonlinear effective optical susceptibility χen, a spatially uniform pump electric field (i.e. pump wave vector k0≈0)xE0exp⁡(-iω0t ) is applied to semiconducting plasma. The classical hydrodynamic model of homogeneous semiconductor plasma of infinite extent (i.e.kl≪1, k is the wave number of the acoustic wave and l the mean free path of the electron) has been extended to include essential quantum corrections resulting in one component quantum plasma described by the QMHD model.

“When plasma is cooled to an extremely low temperature, the de Broglie wavelength of the charge carriers can be comparable to the dimensions of the system. In such situations, ultra-cold plasma behaves like a Fermi gas, and quantum mechanical effects are expected to play a central role in the behavior of charged particles” [22].

∂υ0∂t+νυ0=-emE0+v0×B0               							(1)

∂υ1∂t+νυ1+υ1υ0∂∂x=-emE1+υ1×B1-1mn0∂P∂x+FQ				(2)

Where,   FQ=2μBℏm∇B1.Sα+ℏ24m2n∂3n1α∂x3

υ0∂n1α∂x+n0∂υ1∂x+∂n1α∂t= 0        		(3)

∂E1∂x+n1αeε=βε∂2u∂x2                                          	(4)

ρ∂2u∂t2+2γsρ∂u∂t+β∂E1∂x=C∂2u∂x2                   	(5)

Equation (1) and (2) describe the electron motion of the fields associated with the pump and the side band waves under the influence of a magnetostatics field, respectively. B0,v0 and B1,v1 are the equilibrium and perturbed magnetic fields and oscillatory fluid velocities of the electrons of effective mass m and charge e.The effect due to v0×B1 is neglected in this study by assuming that the acoustic wave is propagating along such a direction of the crystal as to produce a longitudinal electric field and spin states of the particles will be perturbed by the presence of EM waves. The P represents the degenerate pressure P=mVFα2n1α5/35n0α2/3, where VFαj=ξ3Dℏ(n0α1/3)m is the Fermi velocity. ξ3D is the degree of spin-polarization given by ξ3D=1-η5/3+1+η5/3/2 with spin polarization (η) defined by η=n↑-n↓/n↑+n↓. The quantum force FQ on an electron in Eq. (2) includes two terms. The first term represents the Bohm potential associated with quantum diffusion of electrons and the second term is the spin magnetization energy due to the spin interaction with magnetic field. Here Sα is the spin of species α, α=↑and↓ denotes the spin up and spin down electrons respectively with μ=-gμB2,μB=eℏ2m,g=2.0023192 is the electron g factor,  n1α is the perturb number density of species α. It is well known that the linearly polarized transverse electromagnetic wave is not affected by the quantum effects.

∂2n1α∂t2+ω2pn1α+n02μBℏmik2Eω0Sα0+βε∂2u∂x2+ν∂n1α∂t=  E∂n1α∂x		(6)

Where E=emE0(1+ωc ν-iω0ωc2-ω02-2iω0ν)

In the derivation of Eq. (6), we have neglected the Doppler shift under the assumption that ω0≫v>kυ0;ωp=n0e2mε12, ω2pis the modified plasma frequency strongly influenced by Bohm potential and Fermi Pressure. The quantum forces and Fermi Pressure both are included in the second term on LHS of eq. (6). In further calculations authors shall study the combined effect of both the quantum correction terms. The perturbed electron concentration n1α has two components, known as  fast  and slow n1α=nf+ns.The slow component ns (viz.,ns∝expi(ksx-ωst)) is associated with the phonon mode (ωs,ks) and the fast component nf (viz.,nf∝expi(k1x-ω1t)) is associated with  the high frequency scattered electromagnetic wave (ω1,k1), arising due to the three wave parametric interaction.These waves will propagate at generated frequencies ωs and ω0±ω1respectively. We assume that the energy transfer between the pump and produced signal and idler waves satisfy phase matching conditions which are ω0=ω1-ωs and k0=k1-ks. Now for spatially uniform laser radiationk0≈0, one obtainedk1=ks=k. By resolving Eq. (6) into two components (fast and slow) under the rotating wave approximation, we obtain the respective coupled equations as

∂2nαf∂t2+v∂nαf∂t+ωp2nαf=E∂n*αs∂x                 	 			(7a)

∂2nαs∂t2+ω2pnαs+n02μBℏmik2Eω0Sα0+βε∂2u∂x2+ν∂nαs∂t=  E∂n*αf∂x  			(7b)

Subscript s and f stand for slow and fast components, respectively. Asterisk (*) represents complex conjugate of the quantity.  We restrict our analysis only for the Stoke’s component (ω0-ωs) of the scattered electromagnetic waves. It is inferred from eq. (7) that the slow and fast components of the density perturbations are coupled to each other via the pump electric field. Thus, the presence of the pump field is a fundamental necessity for parametric interactions to occur. From Eq.(7a), (7a), and (5), we get.

n=n0(2μBℏmik2Eω0Sα0+eβmε∂2u∂x2) (δ12 -iωsv - k2E2δ22+ iω1v )                    (8)

The number density of our expected piezoelectric quantum plasma medium is influenced by both spin-up and spin-down species and quantum Bohm potential and component of piezoelectricity. Now here we also clarified our analysis by assuming that the medium is sufficiently cooled, the temperature is below Fermi temperature, and the degenerate plasma state is reached [17].

s↑0=-s↓0=ℏ2z and  n↑-n↓=3nμBB02kBTF (T≪TF).

These assumptions allowed us to focus on the key interactions and behaviours of the particles in the system, providing a clearer understanding of the overall dynamics. The effect of spin electrons in the Stoke’s component of induced current density is given by.

J1=-n*ev0     								(9)

Substituting Eq. (8) into Eq. (9) we get

J1=E0EεωP2v-iω0(ωc2-ω02-2iω0v)eβ2k3mεργsωs-2μBℏmik2E*ω0Sα0[ δ12+iωsv-k2E2δ22-iωsv]-1	(10)

δ12=ωp2-ωs2  and   δ22=ωp2-ω12,   ω0=ω1-ωs and v0x=E(v-iω0)

The components of oscillatory electron fluid velocity v0 are obtained from eq. (1). Henceforth, treating the induced polarization P1 as the time integral of J1, we can write P1=J1dt. Using this approach, we obtain the nonlinear induced polarization due to the perturbed density.

P1=-iω0E0E1εωP2v-iω0(ωc2-ω02-2iω0v)eβ2k3mεργsωs-2μBℏmik2ω0Sα0  [ δ12+iωsv-k2E2δ22-iωsv]-1   (11)

Now the second-order polarization is defined as

P1=ε0χe2E0E1				 (12)

Using equation (11) and (12) the Second order nonlinear susceptibility is as follows.

χe2=-iω0ε0 εωP2v-iω0(ωc2-ω02-2iω0v)eAkmγsωs2-2μBℏmik2ω0Sα0[ δ12+iωsv-k2E2δ22-iωsv]-1	 (13)

It is evident from equation (13) that the second-order nonlinear susceptibility χe2 (via P1) is a complex quantity, that includes real and imaginary parts. The imaginary parts can be employed to steady state growth and gain characteristics, while the real part is used to explore the dispersion characteristics of the medium. The steady-state gain coefficient of the parametrically excited waveform of the pump field exceeding the threshold value is obtained through the relation [23].

gQ=-k2ε1[χe2]iE0  								(14)

3. results and discussion

In this section, the author analytically studies second-order nonlinearity by employing the QMHD model for the electron dynamics in the semiconductor plasma. The electron dynamics in the semiconductor is highly influenced by the external magnetic field and spin plays a vital role in exposing the plasma to an external magnetic field, which interacts with the magnetization in the plasma due to the electron spin.  To the best of the author's knowledge, no work has been done to observe the spin effect in parametric interaction in semiconductor plasmas. The numerical estimations have been made for n-type InSb assumed to be duly irradiated by pulsed 10.6μm CO2 laser at 77 k.The physical parameters used are: m=0.107m0,ε1=9.35,vs=1.8×103ms-1, β=0.21Cm-2,ρ=4.82×103kgm-3, ωs=2×1011s-1,ω0=1.78×1014s-1,ν=5×1013s-1,n0=2×1024m-3,TF=77K.

β=0.21Cm-2,ρ=4.82×103kgm-3,ωs=2×1011s-1,ω0=1.78×1014s-1,ν=5×1013s-1,n0=2×1024m-3,TF=77K.Using the above parameters, we have studied the spin effect in optical parametric dispersion and amplification characteristics originated by real and imaginary part of optical χe2 respectively. The optical susceptibility of the medium χe2 is depends on the different parameters like wave vector (k), pump amplitude (E0), number density n0 and magnetic field (B0). The parametric gain of the generated acoustic wave requires the pump field to exceed a certain threshold value.

As an illustration, Fig. 1 shows the dependence of gain constant with the pump amplitude E0. The gain constant increases linearly with the pump amplitude E0 indicating a direct relationship between the two variables. This graph demonstrates how changes in pump amplitude directly impact the gain constant in the system. It is also found that gain constant for parametric amplification is affected by the spin effects. The solid, dashed line showed the variation for fully spin-polarized (η=1) and partially spin-polarized (η=0.5) respectively. In this case, amplification decreases with increasing spin-polarization. It is observed that in both cases gain constant increases with increasing value of E0and Spin effects sufficiently increase the required gain constant to an appreciable extent.

Fig.1: Variation of gQ with pump amplitude E0 at  ωc=1.75×1018s-1 and n0=2×1018m-3.

Fig.2. Variation of Gain constant gQ  with number density n0 at   E0=6×107m-1  and  k=6×107m-1.

Fig. 2, depicts the variation of gain constant with free carrier density n0. It is found that the doping concentration significantly alters the nonlinear susceptibility of the semiconductor medium. It may be inferred that gain reduces parabolically with increases in carrier density. The solid, dashed line showed the variation for fully polarized (η=1) and partially polarized (η=0.5) respectively and in this case, amplification increases with increasing spin-polarization.

Fig.3. Variation of Gain constant  gQ with wave vector k k  at  E0=6×107m-1 and n0=2×1024m-3n0=2×1018m-3 .

Fig. 3 illustrates the variation of gain constant gQ with wave vector k. In both cases gain constant decreases on increasing k. The fully spin-polarization is found to decrease the magnitude of gain constant. The dependence of the gain constant on the wave vector in the regime of large particle concentration and large magnetic field. Large concentration allows to reach large magnetization and rather small wavelengths. Increasing the external magnetic field increases the cyclotron frequency and the resonance frequency.

The real part of optical susceptibility leads to the properties of the dispersion relation of the medium. The wide range of doping concentrations results in a correspondingly wide range of nonlinear optical properties, making it a versatile material for various applications in photonics and optoelectronics.

Fig.4. Variation of Real χe2 with plasma frequency modified by number density k p/c  at  E0=6×107m-1 and k=6×107m-1.

As an illustration, Fig. 4 illustrates the variation of the real part of susceptibility with number density via normalized frequency. The nature of both curves is the same, showing an increase in susceptibility with increasing number density that reaches a higher value and then, starting, decreases as frequency increases. This behavior indicates a critical point where the susceptibility reaches a maximum value before decreasing. The relationship between number density and susceptibility is crucial for understanding the material's response to external applied fields. The solid, dashed line showed the variation for fully polarized (η=1) and partially polarized (η=0.5) respectively. The nature of both curves is the same, but with the fully spin-polarized, medium reaching a higher maximum susceptibility compared to the partially spin-polarized. This distinction highlights the impact of polarization on the material's response to external fields. Overall, the behaviour of the medium in response to external fields is directly influenced by the level of spin-polarization present. Understanding this relationship is essential for predicting and manipulating the material's susceptibility in various applications.

Fig.5. Variation of Real χe2 with cyclotron frequency k c/0  at  E0=1×108m-1 and k=1×108m-1.

As an illustration, Fig. 5 illustrates the variation of the real part of susceptibility with cyclotron frequency k c/0 which depends on the externally applied magnetic field. Spin plays a vital role in exposing the plasma to an external magnetic field, which interacts with the magnetization in the plasma due to the electron spin. The solid, dashed line showed the variation for fully polarized (η=1) and partially polarized (η=0.5) respectively. The nature of both curves is the same, but with the partially spin-polarized, medium reaching a higher susceptibility compared to the fully spin-polarized. In magnetized plasmas, electrons align their spin along the external magnetic field, which enhances the strength of the external magnetic field. This alignment of spin leads to an increase in the overall magnetic properties of the plasma. In the analysis, the magnitude of the real part of second-order susceptibility is found to be of the order of 1.96×10-10 SI units while considering s↑0=-s↓0 and n=n↑-n↓=3nμBB02kBTF   with carrier density n0=1024m-3.

4. Conclusion

Based on the above discussions, the following conclusions may be drawn:

- This analysis established that the spin properties of electrons may be studied by employing a quantum hydrodynamic (QMHD) model via quantum correction, including Fermi pressure, Bohm potential, and spin effect in optical parametric processes.

- It establishes that the spin of electrons plays a crucial role in exposing the plasma to an external magnetic field and modifies the dispersion characteristics. These modified dispersion characteristics can lead to changes in transport properties and increase the overall magnetic properties of the plasma.

- The magnetic properties of any medium depend on the number of unpaired electrons and how they interact with one another. In our analysis, this spin-polarization plays a crucial role in the understanding of the behaviour of semiconductor plasma in the presence of an external field.

- It is found that the magnitudes of the threshold electric field for the onset of parametric amplification are 9.109×106 Vm-1 (4.296×1011Wm-2) which is easily obtainable frequency-doubled CW and pulsed 10.6 µm CO2 lasers.

- The calculated value of second-order optical susceptibility (Imaginary and Real part) agrees well with values theoretically quoted by Shen [36] using band-charge model and empirical pseudo-potential method. Those quoted values of Shen [24] are in fair agreement with experimental values [25].

Disclaimer (Artificial intelligence)

Option 1:

Author(s) hereby declare that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc.) and text-to-image generators have been used during the writing or editing of this manuscript.

Option 2:

Author(s) hereby declare that generative AI technologies such as Large Language Models, etc. have been used during the writing or editing of manuscripts. This explanation will include the name, version, model, and source of the generative AI technology and as well as all input prompts provided to the generative AI technology

Details of the AI usage are given below:

1.

2.

3.

References

- Brodin, G., Marklund, M., & Manfredi, G. (2008). "Quantum plasma effects in the classical regime." Phys. Rev. Lett., 100, 175001.

- Brodin, G., & Marklund, M. (2007). "Spin magnetohydrodynamics." New J. Phys., 9, 277.

- Shahid, M., Usmani, S., Iqbal, Z., Hussain, A., & Bukhari, S. (2022). "Drifts effect on the ordinary plasma wave and the existence of new spin dependent electron drift in the spin quantum plasma." Phys. Plasmas, 29, 062107.

- Shahid, M., Melrose, D. B., Jamil, M., & Murtaza, M. (2012). "Spin effect on parametric interactions of waves in magnetoplasmas." Phys. Plasmas, 19, 112114.

- Han, D., & Jung, Y. D. (2011). "Spin effects on the instability and propagation modes of electrostatic plasma waves in quantum plasmas." Appl. Phys. Lett., 99, 121506.

- Shukla, P. K., Shukla, N., & Stenflo, L. (2010). "Generation of magnetic fields by the ponderomotive force of electromagnetic waves in dense plasmas." J. Plasma Phys., 76, 25.

- Shukla, P. K., & Stenflo, L. (2006). "Stimulated scattering instabilities of electromagnetic waves in ultracold quantum plasma." Phys. Plasmas, 13, 044505.

- Ren, H., Wu, Z., & Chu, P. K. (2007). "Dispersion of linear waves in quantum plasmas." Phys. Plasmas, 14, 062102.

- Iqbal, Z., & Murtaza, G. (2018). "Nonlinear analysis of obliquely propagating spin electron acoustic waves in a partially spin polarized degenerate plasma." Phys. Lett. A, 382, 44–48.

- Stefan, M., Brodin, G., Haas, F., & Marklund, M. (2010). "Effects of the electron spin on the nonlinear generation of quasi-static magnetic fields in a plasma." J. Plasma Phys., 76, 865.

- Stefan, M., & Brodin, G. (2013). "Linear and nonlinear wave propagation in weakly relativistic quantum plasmas." Phys. Plasmas, 20, 012114.

- Brodin, G., Lundin, J., Zamanian, J., & Stefan, M. (2011). "Nonlinear wave interaction and spin models in the magnetohydrodynamic regime." New J. Phys., 8, 083017.

- Ghosh, S., Dubey, S., & Vanshpal, R. (2013). "Steady state and transient gain characteristics of the stimulated Brillouin scattered mode in quantum semiconductor plasmas." Chin. J. Phys., 51, 6.

- Stefan, M., Brodin, G., & Marklund, M. (2010). "Spin-induced nonlinearities in the electron magnetohydrodynamic regime." New J. Phys., 12, 013006.

- Brodin, G., Marklund, M., Zamanian, J., & Stefan, M. (2011). "Spin and magnetization effects in plasmas." Plasma Phys. Control. Fusion, 53, 074013.

- Guha, S., Sen, P. K., & Ghosh, S. (1978). "Parametric instability of acoustic waves in transversely magnetized piezoelectric semiconductors." Phys. Stat. Sol. (a), 52, 407.

- Hu, Q. L., Zhou, S. L., Yu, X. G., & Xiao, G. L. (2016). "Spin effects on the EM wave modes in magnetized plasmas." Phys. Plasmas, 23, 11.

- Chen, S., Li, C., Zha, X., Zhang, X., & Xia, Z. (2020). "High-frequency surface waves in quantum plasmas with electrons relativistic degenerate and exchange-correlation effects." Chin. J. Phys., 68, 1.

- Majedi, S., Khorashadi-Zadeh, S. M., & Niknam, R. A. (2018). "Parametric study of quantum effects in plasmas." Eur. Phys. J. Plus., 133, 2.

- Manfredi, G. (2005). "How to model quantum plasmas." Fields Inst. Commun., 46, 263–287.

- Haas, F., Garcia, L. G., Goedert, J., & Manfredi, G. (2003). "Quantum ion-acoustic waves." Phys. Plasmas, 10, 3858.

- Ghosh, S., Dubey, S., & Vanshpal, R. (2010). "Quantum effect on parametric amplification characteristics in piezoelectric semiconductors." Phys. Lett. A, 375, 43–47.

- Yariv, A. (1975). Quantum Electronics (2nd ed.). New York: Wiley.

- Shen, Y. R. (1984). The Principles of Nonlinear Optics. New York: John Wiley & Sons.

- Fond, C. Y., & Shen, Y. R. (1975). "Theoretical studies on the dispersion of the nonlinear optical susceptibilities in GaAs, InAs, and InSb." Phys. Rev. B, 12, 2325.