Case report

SELECTIVE REMOVAL OF DENTAL CARIES WITH BIOACTIVE GLASS 45S5 JET: A CASE REPORT

.

ABSTRACT

Aims: This case report aims to demonstrate the clinical application and effectiveness of bioactive glass 45S5 air-abrasion as a selective caries removal technique prior to adhesive restoration. The approach prioritizes dentin preservation, promotes remineralization, and contributes to the longevity and quality of the restorative outcome. Presentation of Case: A patient presented to the dental clinic with active carious lesions on the occlusal and buccal surfaces of posterior teeth. Clinical and radiographic examinations confirmed the presence of dentin caries without pulpal involvement. The carious tissue was selectively removed using bioactive glass 45S5 air-abrasion, preserving affected dentin near the pulp while maintaining sound peripheral dentin and enamel for optimal sealing. Following caries removal, an adhesive system was applied, and the teeth were restored using composite resin. The treatment resulted in excellent aesthetic and functional outcomes, with no postoperative sensitivity or complications reported. Discussion: The management of dental caries has shifted toward minimally invasive strategies that preserve healthy dental structures. Selective caries removal, when combined with bioactive materials like bioactive glass 45S5, offers additional benefits such as dentin remineralization and improved restoration longevity. Although the literature supports the remineralizing potential of 45S5 bioactive glass, its influence on adhesive bond strength remains under investigation. In this case, the technique proved clinically effective, suggesting that air-abrasion with bioactive glass can be a viable adjunct in conservative caries management. Conclusion: This case highlights the effectiveness of bioactive glass 45S5 air-abrasion in selective caries removal, providing a predictable, conservative, and biologically favorable approach. The technique supported functional and aesthetic restoration without postoperative sensitivity, reinforcing its potential as a valuable tool in contemporary restorative dentistry.

Keywords: Bioactive glass, Selective Removal, Caries.

1. INTRODUCTION

Dental caries is the most prevalent non-communicable disease encountered in dental clinics. It is characterized as a biofilm-sugar-dependent disease, resulting from an imbalance in the demineralization/remineralization process that affects dental structures—namely enamel, dentin, and cementum, due to the acids produced by the metabolic activity of the dental biofilm on dietary sugars (Batista, Vasconcelos, & Vasconcelos, 2020).

According to Nigel et al. (2017), the frequent intake of dietary carbohydrates leads to the overproduction of acids and selects for acidogenic and aciduric bacterial species. As a result of this imbalance, the disease manifests clinically in its early stages as active white spot lesions in the enamel or, in more advanced stages, as dentin cavitations and/or pulp necrosis. Therefore, effective caries management is directly related to the patient’s adherence to behavioral changes and the appropriate indication of clinical interventions (Large et al., 2023).

According to Silva et al. (2017), therapeutic approaches in cariology can be classified into three groups. The first group comprises invasive approaches, which involve the selective removal of carious tissue using manual and/or rotary instruments, and are commonly followed by restorative protocols, preferably with adhesive materials such as burs and curettes. The second group includes microinvasive techniques, which aim to avoid unnecessary tissue removal and preserve tooth structure for as long as possible. These include sealants, resin infiltration, and bioactive glass air-abrasion (Sheiham & James, 2015). Finally, the third group involves non-invasive approaches, which do not include any tissue removal, such as sugar intake control, biofilm management, and the use of fluoride or other remineralizing agents (Inchingolo et al., 2023).

In line with Minimally Invasive Dentistry (MID) principles, Tumenas et al. (2014) emphasize the preservation of sound hard dental tissues and the minimization of unnecessary alterations. Currently, partial caries removal, aimed at maintaining pulp vitality, is considered the treatment of choice for acute and deep carious lesions—provided that appropriate diagnostic principles are respected. This approach significantly reduces the risk of pulp exposure and postoperative pulp symptoms. Additionally, gradual excavation techniques provide a favorable environment for pulp healing and dentin formation, contributing to a better prognosis (Clarkson et al., 2021).

Bioactive glass air-abrasion has gained significant attention as it is a promising approach for inducing dentin remineralization and improving restoration longevity (Kaimonov & Safronova, 2023). For this technique, bioactive glass 45S5 is used—a calcium/sodium phosphosilicate that reacts with body fluids to induce hydroxyapatite [Ca₁₀(PO₄)₆(OH)₂] formation, according to Bakry et al. (2014). In carious dentin, it can inhibit demineralization, bacterial growth, and the enzymatic activity of matrix metalloproteinases due to the pH elevation promoted by its high ionic release (Lizzi et al., 2017).

This material presents several advantages, including the absence of pain during the more conservative operative procedure, selective removal of infected dentin, and reduced vibration and heat generation. However, it also presents limitations, such as the inability to remove thick carious tissue and defective restorations, the risk of accidental ingestion, and limited tactile feedback (Fernando et al., 2017).

Currently, bioactive glass air-abrasion is employed in dentistry for various procedures, including air polishing, dentin desensitization, enhancing surface free energy and wettability of sandblasted titanium discs (Abushahba et al., 2020), eliminating biofilm from titanium surfaces contaminated with S. mutans, F. nucleatum, and P. gingivalis (Faleh et al., 2019), selectively removing residual orthodontic adhesives without damaging enamel (Taha et al., 2017), enamel white spot lesion remineralization (Milly et al., 2015), and cutting various dental materials (Umair et al., 2017).

The physical properties of bioactive glass suggest it may be effective for selective carious dentin removal. However, current evidence is insufficient regarding the interaction of bioactive glass particles with dentin following caries removal and their effect on the longevity of adhesive systems and restorations (Mocquot et al., 2020).

Therefore, the objective of the present work is to report a clinical case demonstrating the technique and effectiveness of bioactive glass 45S5 air-abrasion for the selective removal of carious tissue prior to composite resin restoration.

2. PRESENTATION OF CASE

A 21-year-old male with light skin (leucoderma), presented to the Restorative Dentistry Clinic of Paulo Picanço Faculty – FACPP with the chief complaint of "the need for restorations." During the anamnesis and medical history review, no systemic conditions, pain, or sensitivity were reported.

Intraoral clinical examination revealed a white spot lesion with early cavitation on the main fissure of tooth 46, and in tooth 47, a brown discoloration in both the primary and secondary fissures, along with a subtle white spot lesion surrounding an amalgam restoration on the buccal surface. Additional visual signs included changes in color, opacity, and translucency of the enamel, which clearly outlined areas of alteration (Figure 1).

This study followed the ethical principles and guidelines established by Resolution 466/12 of the Brazilian National Health Council. The participant signed an informed consent form, and the study was approved by the Research Ethics Committee of the Paulo Picanço Faculty for the purpose of conducting this clinical investigation.

As a clinical operative strategy, the proposed treatment plan consisted of the selective removal of carious enamel using 45S5 bioactive glass air-abrasion, followed by adhesive restoration of the affected tooth. The patient was monitored over a period of six months, with clinical progress documented through radiographs, photographs, clinical evaluations, and sensitivity tests.

Fig 1. Initial clinical appearance of teeth 46 and 47.

Fig 2 . Periapical radiographic examination of teeth 46 and 47.

As a complementary examination, a periapical radiograph was requested, which confirmed the presence of dentin caries in the involved teeth (Figure 2).

Fig 3 . Selective removal of infected enamel from teeth 46 and 47.

Following inferior alveolar and buccal nerve block anesthesia with lidocaine hydrochloride and epinephrine (Alphacaine 100, DFL, Rio de Janeiro, Brazil), the coronal opening of tooth 46 was initiated through the occlusal surface using a spherical diamond bur (Invicta FG 1014HL, American Burrs, Porto Alegre, RS, Brazil). Subsequently, coronal access was performed on tooth 47 through both the occlusal and buccal surfaces.

Selective removal of the infected enamel was performed on both teeth using a minimally invasive approach (Figure 3), followed by air-abrasion with 45S5 bioactive glass to further debride the carious tissue and stimulate dentin remineralization (Figure 4).

Fig 4 . Air-abrasion with 45S5 bioactive glass on teeth 46 and 47.

Fig 5 . Final restoration using light-cured composite resin.

The restorative procedure included selective enamel etching with 37% phosphoric acid (All Prime Dental Products, São José, SC, Brazil) for 30 seconds, rinsing with water for 60 seconds, and thorough air-drying. A universal adhesive system (Ambar Universal APS, FGM, Joinville, SC, Brazil) was applied in two active layers: the first applied for 20 seconds followed by 10 seconds of air-drying, and the second for another 20 seconds. Light curing was carried out for 40 seconds using the Optilight D700 unit (Saevo, Cordoba, Argentina).

The cavities were then restored using light-cured composite resin Opallis® (FGM, Joinville, SC, Brazil) in shades A2D and A1E. Finishing was performed using a flame-shaped diamond bur (3118F, KG Sorensen, São Paulo, Brazil), and polishing was completed using the Ultra-Gloss kit (American Burrs, Porto Alegre, RS, Brazil) in combination with Diamond Excel polishing paste (FGM, Joinville, SC, Brazil) (Figure 5).

The patient returned to the Paulo Picanço Faculty for a follow-up evaluation six months after the procedure. A periapical radiograph was taken (Figure 6), along with a clinical photograph of the restored teeth (Figure 7). The restoration was found to be intact and clinically satisfactory, with no signs of failure, and the patient remained asymptomatic.

Fig 6 . Six-month periapical radiograph of teeth 46 and 47.

Fig 7. Clinical photograph of the restoration after six months: The restoration remained satisfactory, with no signs of failure, and the patient reported no symptoms.

3. DISCUSSION AND Conclusion

Dental caries is a complex and dynamic pathological condition with multiple etiologies. Its initiation and progression are primarily controlled by microbial and host-related factors, such as frequent and unbalanced carbohydrate intake (Cantoral et al., 2021). Characterized by an intrinsic relationship between biofilm and dietary sugars, the process involves the fermentation of sucrose by acids and its metabolism into intra- and extracellular polysaccharides by microorganisms present in the biofilm. This leads to a dysbiotic imbalance in the dental structures, resulting in disruptions in the demineralization and remineralization processes (Pham & Nguyen, 2018).

Drancourt et al. (2019) classified the stages of carious lesions based on activity, visual signs, and lesion extent. As caries activity progresses, the lesion environment undergoes modifications that result in progressive mineral loss, evolving from small lesions to increasing levels of structural damage. This process may eventually lead to cavitation and destruction of affected tooth structures. These changes are reflected in clinical features such as surface texture, translucency, and color—parameters crucial for staging the lesion.

Caries typically begins on the tooth surface and can affect the enamel, dentin, and in more severe cases, the dental pulp. The choice of treatment depends on the severity of the lesion. In milder cases where the pulp is not affected, the recommended approach is restorative treatment. This involves direct restorations using composite resin or amalgam. However, these materials may develop marginal defects that can lead to secondary caries (Moussa et al., 2022).

Secondary caries are defined as lesions that develop adjacent to existing restorations, most frequently at the cervical margins. These areas are prone to biofilm accumulation due to issues such as bacterial microleakage, gaps, and marginal defects—particularly in proximal boxes (Pinto et al., 2023). In the clinical case discussed, the patient presented with a white spot lesion around the buccal amalgam restoration on tooth #47, a typical characteristic of secondary caries, which can be clinically indistinguishable from primary caries, as described by Nedeljkovic (2015).

Currently, various therapeutic strategies are employed for caries management, beginning with non-invasive methods such as topical fluoride application, use of fluoridated toothpaste, regular dental visits, and oral health education. When carious tissue is present, the removal of infected dentin becomes necessary (Cury et al., 2016). The conventional technique for selective caries removal involves mechanical instruments such as low-speed steel burs and manual tools like spoon excavators. However, this method carries the risk of removing healthy dentin, depending on the operator's skill—especially when using rotary instruments (Figundio et al., 2023).

An alternative microinvasive approach aims to preserve as much healthy tooth structure as possible, minimizing unnecessary removal. The use of dental sealants protects tooth surfaces, particularly pits and fissures, from caries development. Additionally, air-abrasion with bioactive glass has emerged as a technique that not only selectively removes infected tissue but also promotes remineralization of demineralized enamel in a conservative manner (Bezerra et al., 2018).

Modern operative dentistry embraces a minimally invasive approach, integrating prevention, remineralization, and conservative intervention when placing or replacing restorations. This approach prioritizes the preservation of tooth structure and reduction of unnecessary intervention (Tumenas et al., 2014). Therefore, in the case presented, carious tissue was initially removed using a low-speed handpiece and carbide bur #4, followed by selective removal of deeper infected dentin using 45S5 bioactive glass air-abrasion.

The use of bioactive glass, especially the 45S5 formulation, has gained prominence in dentistry. When applied to the dental substrate, it stimulates remineralization by forming carbonated hydroxyapatite (HCA). With a high bioactivity index, 45S5 bioglass adheres well to both hard and soft tissues and demonstrates excellent biocompatibility (Zhang et al., 2021). It also promotes remineralization of enamel and dentin with low cytotoxicity to pulp cells and possesses notable antimicrobial properties (Rehab et al., 2022).

In caries-affected dentin, bioactive glass may form a mineral-rich “bioactive smear layer” that promotes dentin remineralization. The interaction between bioactive glass and body fluids supports the deposition of hydroxyapatite and repair of dental hard tissues. Moreover, air-abrasion with bioactive glass results in rounded internal cavity angles, which reduce composite polymerization shrinkage stress, minimize patient discomfort, and enable selective carious dentin removal (Ramadoss, Padmanaban, & Subramanian, 2021).

Wu et al. (2020) investigated the remineralization effects of 45S5 bioactive glass on artificially induced dentin caries. Their findings demonstrated significant increases in surface microhardness and the formation of a remineralized zone. The particles of 45S5 adhered to dentin and facilitated the formation of a hydroxyapatite layer with a structure similar to dental enamel and dentinal tubules (Salah et al., 2022).

After caries removal, the next critical step is restoration. This begins with the application of phosphoric acid, which demineralizes the dentin to expose collagen fibers and enhances micromechanical retention of the resin composite. The hybrid layer formation aims to infiltrate these interfibrillar spaces. However, excessive exposure of collagen may lead to hydrolysis and collapse of the fibrils, compromising the adhesive interface and promoting gap formation (Bakry et al., 2014).

Cavity preparation is, therefore, essential. The prior use of bioactive glass not only aids in selective caries removal but also facilitates the creation of rounded internal cavity contours, minimizing polymerization stress (Frazão et al., 2015). In the clinical case described, selective caries removal using 45S5 bioactive glass air-abrasion provided a pain-free, comfortable procedure that supported the stability and longevity of the final composite restorations.

Competing interests

The authors declare that they have no conflicts of interest related to this study.

References

ABUSHAHBA, F.; SÖDERLING, E.; AALTO‐SETÄLÄ, L.; HUPA, L.; NÄRHI, T. Air Abrasion with Bioactive Glass Eradicates Streptococcus mutans Biofilm from a Sandblasted and Acid-Etched Titanium Surface. Journal of Oral Implantology, v. 45, n. 6, p. 444–50, 2019.

ABUSHAHBA, F.; TUUKKANEN, J.; AALTO‐SETÄLÄ, L.; MIINALAINEN, I.; HUPA, L.; NÄRHI, TO. Effect of bioactive glass air‐abrasion on the wettability and osteoblast proliferation on sandblasted and acid‐etched titanium surfaces. European Journal of Oral Sciences, v. 128, n. 2, p. 160–9, 2020.

BAKRY, AS.; TAKAHASHI, H.; OTSUKI, M.; TAGAMI, J. The effect of a bioglass paste on enamel exposed to erosive challenge. J Dent, v. 42, 2014; 1458-63.

BAKRY, AS; TAKAHASHI, H; OTSUKI, M; TAGAMI, J. Evaluation of new treatment for incipient enamel demineralization using 45S5 bioglass. Dental Materials, v. 30, n. 3, p. 314–20, mar. 2014.

BEZERRA, NVF.; MORAIS, WA.; SALMA, R.; SALES, EMA.; VICTOR PINHEIRO FEITOSA; AZEVEDO, K. Efeito da Associação de Profilaxia com Biovidro Fluoretado e Aplicação Tópica de Flúor na Remineralização do Esmalte. Journal of Health Sciences, v. 19, n. 5, 23 fev. 2018; 125–5.

CANTORAL, A.; MUÑOZ-ROCHA, Teresa Verenice.; LUNA-VILLA, Lynda Cristina.; MANTILLA-RODRÍGUEZ, Andrés.; UREÑA-CIRETT, José Luis.; CASTIBLANCO, Gina Alejandra., et al. Association of Dietary Fluoride Intake and Diet Variables with Dental Caries in Adolescents from the ELEMENT Cohort Study. Caries Research, v. 55, n. 2, p. 88–98, jan. 2021.

CLARKSON, JE; RAMSAY, CR; RICKETTS, D; BANERJEE, A; DEERY, C; LAMONT, T, et al. Selective Caries Removal in Permanent Teeth (SCRiPT) for the treatment of deep carious lesions: a randomised controlled clinical trial in primary care. BMC oral health, v. 21, n. 1, 9 jul. 2021.

CURY, JA.; DE OLIVEIRA, BH.; DOS SANTOS, APP.; TENUTA, LMA. Are fluoride releasing dental materials clinically effective on caries control? Dental Materials, v. 32, n. 3, mar. 2016; 323–33.

DRANCOURT, N.; ROGER-LEROI, V.; MARTIGNON, S.; JABLONSKI-MOMENI, A.; PITTS, N.; DOMÉJEAN, S. Carious lesion activity assessment in clinical practice: a systematic review. Clinical Oral Investigations, v. 23, n. 4, p. 1513–24, fev. 2019.

FERNANDO, D.; ATTIK, N.; PRADELLE-PLASSE, N.; JACKSON, P.; GROSGOGEAT, B.; COLON, P. Bioactive glass for dentin remineralization: A systematic review. Materials Science and Engineering: C, v. 76, p. 1369–77, jul. 2017.

FIGUNDIO, N.; PEDRO CAMPOS LOPES; TAMARA KERBER TEDESCO; CAMPOS, J.; VICENTIS, G.; CAROLINA, A. Deep Carious Lesions Management with Stepwise, Selective, or Non-Selective Removal in Permanent Dentition: A Systematic Review of Randomized Clinical Trials. Healthcare, v. 11, n. 16, 18 ago. 2023; 2338–8.

FRAZÃO, Mayara Cristina Abas et al. Biovidro 45S5: um avanço biotecnológico nos materiais restauradores da odontologia. Revista da Faculdade de Odontologia de Lins, v. 25, n. 2, p. 47-55, 2015.

INCHINGOLO, AM; INCHINGOLO, AD; LATINI, G; GAROFOLI, G; SARDANO, R; DE LEONARDIS, N, et al. Caries prevention and treatment in early childhood: comparing strategies. A systematic review. European Review for Medical and Pharmacological Sciences, v. 27, n. 22, p. 11082–92, 1 nov. 2023.

KAIMONOV, MR; SAFRONOVA, TV. Materials in the Na2O-CaO-SiO2-P2O5 System for Medical Applications. Materials (Basel), v. 16, n. 17, 31 ago. 2023.

LARGE, J; MADIGAN, C; PRADEILLES, R; MARKEY, O; BOXER, B; ROUSHAM, EK. Impact of unhealthy food and beverage consumption on children’s risk of dental caries: a systematic review. Nutrition Reviews, 12 dez. 2023.

LIZZI, F.; VILLAT, C.; ATTIK, N.; JACKSON, P.; GROSGOGEAT, B.; GOUTAUDIER, C. Mechanical characteristic and biological behaviour of implanted and restorative bioglasses used in medicine and dentistry: A systematic review. Dental Materials, v. 33, n. 6, p. 702–12, jun. 2017.

MILLY, H.; FESTY, F.; ANDIAPPAN, M.; WATSON, TF.; THOMPSON, I.; BANERJEE, A. Surface pre-conditioning with bioactive glass air-abrasion can enhance enamel white spot lesion remineralization. Dental Materials, v. 31, n. 5, p. 522–33, maio 2015.

MOCQUOT, C.; ATTIK, N.; PRADELLE-PLASSE, N.; GROSGOGEAT, B.; COLON, P. Bioactivity assessment of bioactive glasses for dental applications: A critical review. Dental Materials, v. 36, n. 9, p. 1116–43, set. 2020.

MOUSSA, DG.; AHMAD, P.; MANSOUR, TA.; SIQUEIRA, WL. Current State and Challenges of the Global Outcomes of Dental Caries Research in the Meta-Omics Era. 17 jun. 2022.

NEDELJKOVIC, I.; TEUGHELS, W.; DE MUNCK, J.; VAN MEERBEEK, B.; VAN LANDUYT, KL. Is secondary caries with composites a material-based problem? Dental Materials, v. 31, n. 11, nov. 2015; e247–77.

PHAM, TAV.; NGUYEN, PA. Factors related to dental caries in 10‐year‐old Vietnamese schoolchildren. International Dental Journal, v. 69, n. 3, p. 214–22, nov. 2018.

PINTO, NS.; JORGE, GR.; VASCONCELOS, J.; PROBST, LF.; DE-CARLI, AD.; FREIRE, A. Clinical efficacy of bioactive restorative materials in controlling secondary caries: a systematic review and network meta-analysis. BMC oral health, v. 23, n. 1, 15 jun. 2023; 394.

PITTS, NB; ZERO, DT; MARSH, PD; EKSTRAND, K; WEINTRAUB, JA; RAMOS-GOMEZ, F, et al. Dental caries. Nature Reviews Disease Primers, v. 3, n. 1, 25 maio 2017.

RAMADOSS, R.; PADMANABAN, R.; SUBRAMANIAN, B. Role of bioglass in enamel remineralization: Existing strategies and future prospects—A narrative review. Journal of Biomedical Materials Research Part B: Applied Biomaterials, v. 110, n. 1, 10 jul. 2021; 45–66.

RAMON, Marcelo Gadelha Vasconcelos; VASCONCELOS, Rodrigo Gadelha Vasconcelos. Fisiopatologia da cárie dentária: Entendendo o processo carioso. Revista Salusvita, v. 169–87, 2020.

SALAH, R.; AFIFI, RR.; KEHELA, HA.; ALY, NM.; RASHWAN, M.; HILL, RG. Efficacy of Novel Bioactive Glass in the treatment of Enamel White Spot Lesions: A Randomized Controlled Trial. Journal of Evidence-Based Dental Practice, v. 101725, mar. 2022.

SALMA, REHAB SAMIR; EL DARIDRY, NOUR KHALED; ELMADDAH, HAYA AYMAN; ISMAIL, HODA AHMED; E, SALEM. Comparative analysis of the effect of Bioactive Glass 45S5 on enamel erosion progression in human dentitions (in vitro study). 25 nov. 2022.

SHEIHAM, A; JAMES, WPT. Diet and Dental Caries. Journal of Dental Research, v. 94, n. 10, p. 1341–7, 2015.

SILVA, EL; JANUÁRIO, MVS; VASCONCELOS, MG; VASCONCELOS, RG. Abordagem terapêutica em lesões cariosas: quando e como tratar. Revista Brasileira de Ciências da Saúde, v. 21, n. 2, p. 173–80, 2017.

TAHA, AA.; HILL, RG.; FLEMING, PS.; PATEL, MP. Development of a novel bioactive glass for air-abrasion to selectively remove orthodontic adhesives. Clinical Oral Investigations, v. 22, n. 4, p. 1839–49, 2017.

TUMENAS, I.; PASCO TTOS, R.; JORGE LUIS SAADE; BASSANI, M. Odontologia Minimamente Invasiva. 2014; v. 68, n. 4, p. 283–95.

TUMENAS, I; PASCOTTOS, R; SAADE, Jorge Luis; BASSANI, M. Odontologia Minimamente Invasiva. v. 68, n. 4, p. 283–95, 2014.

UMAIR UL HASSAN, FAROOQ, I.; IMRAN ALAM MOHEET, EMAD AL-SHWAIMI. Cutting efficiency of different dental materials utilized in an air abrasion system. PubMed, v. 11, n. 4, p. 23–7, 2017.

WU, Q., et al. Remineralising effect of 45S5 bioactive glass on artificial caries in dentine. BMC Oral Health, v. 20, n. 1, 11 fev. 2020.

ZHANG, R.; QI, J.; GONG, M.; LIU, Q.; ZHOU, H.; WANG, J., et al. Effects of 45S5 bioactive glass on the remineralization of early carious lesions in deciduous teeth: an in vitro study. BMC Oral Health, v. 21, n. 1, 12 nov. 2021.