Original Research Article

Adsorption of Pb (II) Ions on to Raw Diatomite from Kenya: Equilibrium, Kinetic and Thermodynamics

ABSTRACT

Lead (Pb) is one of the most toxic heavy metals commonly found in industrial effluents discharged into the environment, hence its removal from waste water is essential. In this study, raw diatomite mineral from Kenya was employed in the adsorptive removal of Pb (II) ions from aqueous solutions. The raw diatomite was purified by acid treatment using HNO3 and then it was characterized by X-ray Fluorescence (XRF) and Fourier Transform Infrared Spectroscopy (FT-IR) techniques. XRF data showed that the diatomite was composed mainly of silica. Effect of pH, initial metal ion concentration, contact time, adsorbent dose and temperature on the removal efficiency of Pb (II) ions from aqueous solutions by the raw diatomite was evaluated. The removal efficiency of Pb (II) ions was found to increase with increase in adsorbent dose, contact time and pH but decreased with increasing temperature and initial metal ion concentration. Optimum removal conditions obtained were: pH of 4, 10mg/L initial metal ion concentration, contact time 60 minutes, adsorbent dose of 4g/L and temperature of 25±2°C. The equilibrium was observed to be well described by adsorption isotherms in the order Langmuir > Freundlich> Temkin isotherm model. The adsorption kinetics of Pb (II) ions was described better by pseudo-second -order kinetic model (R2=1), which ascertained that chemisorption was the rate limiting step in the sorption of Pb (II) ions onto raw diatomite. The thermodynamics of the adsorption process indicated that adsorption of Pb (II) ions onto raw diatomite was spontaneous and exothermic in nature. This study demonstrated that raw diatomite from Kenya is effective in heavy metal remediation even without chemical or thermal modifications, therefore, it acts as a promising adsorbent for heavy metal remediation.

Keywords: Lead, diatomite, Kariandusi, Nakuru County, Kenya, Langmuir, Freundlich, Temkin.

1. INTRODUCTION

Heavy metals are toxic pollutants that pose a significant environmental and public health concerns in many parts of the world. In the quest of achieving national development goals, most countries have emphasized on urbanization and industrialization growth at the expense of the environment. Despite the economic benefits, this focus has led to increased pollution, habitat destruction, and a greater risk of environmental hazards (Zulfiqar et al., 2024). The rapid industrialization has led to the indiscriminate discharge of heavy metals and metalloids such as lead (Pb), cadmium (Cd), chromium (Cr), mercury (Hg), arsenic (As) and copper (Cu) into the environment. These heavy metals are toxic even at low concentrations hence their presence in the environment is a subject of great concern (Angon et al., 2024). Unlike organic pollutants, Heavy metals are non-biodegradable, therefore, tend to accumulate in the environment and in animals and plant tissues causing serious health concerns (Tomno et al., 2020).

Lead (Pb) is among the most common heavy metals routinely discharged into the environment due to its prolific use in industrial processes such as manufacture of batteries, paints and coatings, solder, bullets and shot gun shells and electroplating (Arowojobe et al., 2020). Other sources of lead pollution include use of lead-containing pesticides and the discharge of lead containing sludge by wastewater treatment plants. Chronic exposure to lead can cause several unwanted health effects such as damage to the kidneys, cardiovascular system, central nervous system, increased blood pressure, anaemia, infertility in men through sperm damage, miscarriage and stillbirths in pregnant women, stunted growth and diminished learning abilities in children (Ungureanu and Mustatea, 2022). The international agency for research on cancer (IARC) and the US environmental protection agency (USEPA) have classified lead as a probable human carcinogen. Due to its toxicity, the WHO have set the maximum contaminant level (MCL) for lead in drinking water as 0.01mg/L. In Kenya, the national environment management authority (NEMA) has set 0.01mg/L as the maximum allowed limit for discharge of lead into the environment (NEMA, 2006).

Various conventional techniques have been employed in heavy metal remediation such as chemical precipitation, ion exchange and membrane filtration technologies. However, these techniques are complicated, too expensive and require high energy to operate (Abdulwasiu et al., 2022), therefore, they are unsuitable for wastewater remediation especially in developing countries. In addition, chemical precipitation technique produces heavy metal bearing sludge that requires further treatment before discharge into the environment. Although adsorption has proved to be efficient in heavy metal remediation, the high cost of adsorbents such as activated carbon limits its application. Therefore, there is a great need to come up with low-cost adsorbents that replace expensive commercial adsorbents in heavy metal remediation.  As a consequence, researchers have focused on the selection or production of low-cost adsorbents with high adsorption capacities for heavy metals. Industrial waste such as blast furnace slag (Abdelbasir and Khalek, 2022), agricultural waste (Naik et al., 2023) and natural minerals such as Clay minerals (Uddin, 2017) and zeolites (Azizi et al., 2021) have been employed as low-cost adsorbents for heavy metal removal. Among the low-cost adsorbents, natural minerals have gained a lot of interest due to their availability, mechanical and chemical stability, large surface area and cation exchange capabilities.

Diatomite is a soft sedimentary rock of mineral biogenetic origin composed primarily of siliceous skeletal remains of diatoms. It mainly contains silica (SiO2.nH2O) with varying amounts of impurities such as clay, carbonate minerals, iron oxide and organic materials depending on the source (Akafu et al., 2019; Şenol, et al., 2020). Diatomite is of particular interest as an adsorbent due to its unique physiochemical properties such as large surface area, high porosity, high permeability, chemical inertness, fine particle size and low thermal conductivity (Akafu et al., 2019). Studies by Vassileva et al., (2013), Bilgin and Tulun, (2015), Salman et al. (2016) and El Sayed, (2018) have show that diatomite has good adsorption capabilities and is effective in heavy metal remediation. In aqueous solutions, the surface of diatomite has a negative charge due to the dissociation of the surface silanols (Si-OH) groups in the silica matrix, into Si-O‾ and H+ which makes diatomite to have a high affinity for heavy metal cations (Zhao et al., 2019).

Despite Kenya having huge deposits of diatomite mineral in Nakuru and Baringo Counties, the mineral has not been employed extensively in heavy metal remediation in the country. In this study, the adsorption of Pb (II) ions onto raw diatomite from Kenya was investigated. Pb (II) chosen as the preferred heavy metal due to its widespread presence in Kenya’s aquatic environment and industrial effluents. The effect of various adsorption parameters namely: pH, Initial metal ion concentration, contact time, adsorbent dose and solution temperature were investigated. Adsorption isotherms, kinetics and thermodynamic studies were also investigated in order to describe the adsorption process.

2. MATERIALS AND METHODS

2.1 Materials

The powdered raw diatomite sample was obtained from the African Diatomite Industries Limited (ADIL) in Kariandusi, Gilgil, Nakuru County, Kenya. Reagents used in the study were Lead (II) nitrate [Pb(NO3)2; 99%], nitric acid (HNO3; 70%), sodium hydroxide pellets (NaOH, 98%) and deionised water, which were purchased from Sigma-Aldrich. All the reagents were analytical grade and were used as received without further purification.

2.2 Adsorbent Preparation

Adsorbent preparation employed the procedure followed by Zang et al. (2013) with modification. The raw diatomite powder was washed with deionised water five times to remove any adhered impurities, filtered and oven dried at 100ºC for 6 hours. After cooling, 15g of the diatomite sample was placed in a beaker containing 150ml 4M HNO3 acid. The mixture was then placed in an orbital shaker (BioBase SK-0180-Pro) and agitated at 240 rpm for 30 minutes to remove impurities such as calcite that may be present. The diatomite was then filtered through Whatman filter paper No. 40 and washed several times with deionised water until the pH of the rinsing water was 7. The sample was then oven dried at 100ºC for 6 hours.

2.3 Adsorbent Characterization

The chemical composition of the raw diatomite was determined by X-ray fluorescence (XRF) spectroscopy (Empyrean PaNanalytical XRF spectrometer). The infrared spectra (IR) of the raw diatomite was recorded using Fourier transform infrared spectrometer (Shimadzu IRAffinity-1S FT-IR spectrophotometer) in the wave number range 400-4000cm-1 using the KBr pellet technique.

2.4 Batch Adsorption Studies

Batch experiments were carried out to examine the adsorption of Pb (II) ions onto raw diatomite. Experimental parameters namely: initial metal ion concentration (10-70) mg/L; pH (2 to 6), contact time (20-140) minutes; temperature (25 to 65) ºC and adsorbent dosage (0.4-10) g/ L were investigated by changing one parameter at a time while holding the other parameters constant. First, 50 mL Pb (II) ion solutions were prepared in 150 mL plastic bottles via dilution of Pb (II) ions stock solutions with deionised water. The pH of the solutions was monitored using a pH meter (Model HANNA HI 2211) and then it was adjusted by dropwise addition of 0.1 M HNO3 or 0.1 M NaOH solutions. Then, a predetermined amount of raw diatomite was added and the mixture was agitated using an orbital shaker (BioBase SK-0180-Pro) at 240 rpm for 60 minutes. After each run, samples were withdrawn and filtered through Whatman filter paper No. 40. The filtrates were then analyzed for metal ion concentration using Flame Atomic Absorption Spectrophotometer (FAAS) (Model PG 990).

Equations 1 and 2 were used to determine the percentage removal (removal efficiency) and the adsorption capacity, Qe (mg/g) respectively at equilibrium in order evaluate the performance of the raw diatomite as an adsorbent.

| % Removal=(Co-Ce)Co ×100 | (1) |
| --- | --- |
| Qe=(Co-Ce)Vm | (2) |

Where Co and Ce are the initial and equilibrium concentrations (mg/L) of metal ions in the test solution respectively. m is the mass of the adsorbent mass (g), and V is the volume of the test solution used in litres (L).

The adsorption data obtained was applied to Langmuir, Freundlich and Temkin isotherm models while the kinetic experimental data were fitted to pseudo-first-order and pseudo-second order kinetic models. Adsorption thermodynamics were determined by varying the solution temperature from 25 to 65 ºC.

2.5 Adsorption Isotherms

Adsorption isotherms are crucial in describing the adsorption process. Adsorption isotherms relate the amount of adsorbate adsorbed per unit mass of adsorbent (Qe) to the concentration of adsorbate that remains in the bulk solution at equilibrium under constant temperature (Mishra et al., 2017). In this study Langmuir, Freundlich and Temkin isotherm models were applied to describe the adsorption of Pb (II) ions onto raw diatomite.

2.5.1 Langmuir Isotherm

Langmuir isotherm model assumes a monolayer adsorption that is homogeneous exists at all the adsorption sites and there is no interaction between the neighbouring adsorbate molecules (Mustapha et al., 2019). Once a site is filled, no further sorption can take place at that site, hence, the adsorbent surface reaches a saturation point where the maximum adsorption by the surface is achieved (Ajenifuja et al., 2017). Equation 3 represents the linear form of Langmuir isotherm.

| CₑQₑ= 1bQₘ+ CₑQₘ | (3) |
| --- | --- |

Where Cₑ refers to the equilibrium concentration of adsorbate (in mg/l), Qₑ refers to the amount of metal adsorbed per gram of the adsorbent at equilibrium (in mg/g), Qₘ is the maximum monolayer coverage capacity (in mg/g), b is the Langmuir isotherm constant related to the heat of adsorption (in L/mg). The Langmuir parameters Qₘ and b were calculated from the slope and interception of the plot of Cₑ⁄Qₑ against Cₑ. The affinity between the adsorbent and the adsorbate was determined by the use of a dimensionless separation factor, RL whose value indicates the nature of the adsorption process. Equation 4 represents the separation factor, RL.

| R˪=11+bCₒ | (4) |
| --- | --- |

Where Cₒ is the initial concentration (in mg/L) and  b is the Langmuir isotherm constant (in L/mg). The magnitude of the factor indicates whether the adsorption process is unfavourable (RL> 1), linear (RL = 1), favourable (0 < RL< 1), or irreversible (RL = 0) (Etong et al., 2025).

2.5.2 Freundlich isotherm

The Freundlich isotherm accounts for intermolecular interactions between the adsorbate molecules and postulates that adsorbate adsorption takes place on heterogeneous surface through multiyear adsorption. Additionally, it assumes that adsorption takes place in decreasing order of energy, with the stronger binding sites being occupied first and the binding strength decreases as the degree of site occupation increases (Ayawei et al., 2017; Akafu et al., 2019). Equation 5 represents the linearized form of Freundlich isotherm model.

| logQₑ= logKf+ 1nlogCₑ | (5) |
| --- | --- |

Where Qe refers to the amount of metal adsorbed per gram of the adsorbent at equilibrium (in mg/g), Kf refers to the Freundlich constant related to the adsorption capacity, n refers to the Freundlich constant related to the adsorption intensity, Ce refers to the equilibrium concentration of adsorbate (in mg/l). The values of n and Kf were calculated from the slope and intercept respectively of the plot log Qe against log Ce. The n value indicates the degree of non-linearity between solution concentration and adsorption as follows: If n = 1, then adsorption is linear; if n > 1, then adsorption is a physical process: if n < 1, then adsorption is a chemical process (Akinyeye et al., 2016; Mishra et al., 2017).

2.5.3 Temkin Isotherm

The Temkin isotherm accounts for the indirect interaction between the molecules of the adsorbate and implies that adsorption is characterized by a uniform distribution of the binding energies up to a maximum binding energy and that the heat of adsorption of all molecules in the layer decreases linearly with the increase of adsorbent coverage at average concentrations. The isotherm model ignores the extremely low and large concentrations values of the adsorbate (Brazesh et al., 2021). The Linearized form of Temkin isotherm equation is illustrated by equation 6.

| Qₑ=RTbtlnAt+RTbtlnCₑ | (6) |
| --- | --- |

If B=RT/(bt), then equation 6 becomes:

| Qₑ=BlnAt+BlnCₑ | (7) |
| --- | --- |

Where Qe is the adsorption capacity ((mg/g), Ce is the equilibrium concentration of adsorbate (mg/L), At refers to Temkin isotherm binding constant (L/g), bt is the Temkin isotherm constant, B is a parameter related to the heat of adsorption (J/mol); R is the universal gas constant (8.314 J/molK), and T is temperature at 298K (25 ºC). The values for constants At and bt were determined from the intercept and slope, respectively, of the plot of Qe against lnCₑ. If B<8kJ/mol, the adsorption process is a physical adsorption; B>8kJ/mol shows that adsorption is chemical adsorption (Nandiyanto et al., 2022; Ragadhita and Nandiyanto, 2022; Saeed-Ul-Hassan et al., 2024).

2.6 Adsorption Kinetics

Adsorption kinetics are significant in wastewater treatment since they provide valuable insight on the adsorption rate, the adsorption mechanism and also reactions on the adsorbent surface during the adsorption process (Krstić, 2021). The most common kinetic models used to investigate the kinetics of the adsorption process are Lagergren’s pseudo-first-order model and Ho’s pseudo-second-order kinetic models.

2.6.1 Pseudo-First-Order Model

Pseudo-first-order model is based on the assumption that the rate of adsorption is proportional to the number of available sites (Adewale et al., 2024). This model assumes that physisorption is the rate limiting step in the adsorption of particles onto the adsorbent (Liu et al., 2019; Ndung’u, 2021). The pseudo-first-order equation is expressed by equation 8.

| dqtdt=k₁qₑ-qt | (8) |
| --- | --- |

The linearized form of pseudo-first-order model is represented by equation 9.

| Inqₑ-qt=Inqₑ-k₁t | (9) |
| --- | --- |

Where qₑ and qtare the adsorption capacities at equilibrium time and at time t (mg/g) respectively, k₁ is the pseudo-first-order rate constant (min -1) and t is the time (min). The values of k₁ and qe were determined from the slope and intercept of the linear plot of Inqₑ-qt verses t.

2.6.2 Pseudo-Second-Order Model

Pseudo-second-order model is based on the assumption that the rate -limiting mechanism is chemisorption process (Liu et al., 2019). This kinetic model considers that the rate of occupation of the adsorption sites is proportional to the square of the number of unoccupied sites. Pseudo-second-order is expressed by equation 10.

| dqtdt=k₂qₑ-qt² | (10) |
| --- | --- |

The linear form of the model is represented by equation 11.

| tqt=1k₂qₑ²+tqₑ | (11) |
| --- | --- |

Where qₑ and qtare the adsorption capacities at equilibrium time and at time t (mg/g) respectively, k₂ is the pseudo-second-order rate constant (g/mg.min) and t is the time (min). The plot of tqt verses t should gave a straight line and the values of the values of k₂ and qₑ were determined from the intercept and slope respectively.

2.7 Thermodynamic Study

Thermodynamic parameters namely: change in Gibbs free energy (ΔG°), enthalpy change (ΔH°) and entropy change (ΔS°) provide insights into the nature of interactions between the adsorbate and adsorbent, and helps in understanding the feasibility and spontaneity of the adsorption process (Adewale et al., 2024). These parameters were determined using equations 12 – 15.

| ΔG°=-RTlnKC | (12) |
| --- | --- |
| KC=CadsCe | (13) |
| ∆G°=∆H°-T∆S° | (14) |
| lnKC=∆S°R-∆H°RT | (15) |

Where KC is the equilibrium constant, Cads is the adsorbent phase concentration at equilibrium (mg/L), Ce is the equilibrium concentration in the bulk solution (mg/L), R is the universal gas constant (8.314 J/mol/K), T is the absolute solution temperature (K). The magnitude of ΔH° (kJ/mol) and ΔS° (J/mol.K) were determined from the slope and intercept of the Van ’t Hoff plots of lnKC against 1/T respectively. The values of ΔG° (kJ/mol) were determined using equation 12.

The ΔG° values indicate the favourability and spontaneity of the adsorption process. A negative ΔG° value indicates that the adsorption process is feasible and spontaneous at a known temperature. The ΔH° indicates whether adsorption process is exothermic or endothermic in nature. Positive ΔH° values suggest an endothermic adsorption process while a negative ΔH° value correspond to exothermic process (Raji et al., 2023). ΔS° shows disorderliness (randomness) of an adsorbent surface during adsorbent-adsorbate interactions. Positive ΔS° illustrates an increase in the randomness of the adsorption process at the solid-liquid interface while a negative ΔS° indicates decreased randomness (increased order) at the solid-liquid interface (Ndung’u, 2021; Tunceli et al., 2022).

3. RESULTS AND DISCUSSION

3.1 Characterization of the adsorbent

FT-IR spectral analysis was carried out in order to identify the functional groups present in the raw diatomite that might be involved in the adsorption process. The FT-IR spectrum of raw diatomite is presented in Figure 1. The peaks observed at 3463.34cm-1 and 1650cm-1 correspond to stretching and bending vibration modes of -OH groups from physically adsorbed water in the diatomite matrix (Du et al., 2015; Chaudhry et al., 2016). The presence of silica was verified by peaks at 1088.86cm-1 and 476.44cm-1 which were attributed to siloxane (Si-O-Si) asymmetric stretching and bending vibration modes respectively. In addition, the absorption bands at 618.21cm-1 and 719.81cm-1 correspond to stretching vibrational modes of Al-O-Si bond in diatomite (Akafu et al., 2019). The weak peaks at 2926.14cm-1 and 2859.59cm-1 were ascribed to asymmetric and symmetric stretching of the alkyl (C–H) group respectively while the peak at 2013.77cm-1 was ascribed to stretching of the C≡C group. These peaks were as a result of the presence of organic matter impurities in the raw diatomite (Zhang et al., 2019).

Figure 1: Shows the FT-IR spectrum of raw diatomite.

The chemical composition of the raw diatomite was obtained by X-ray Fluorescence Spectrometer. The XRF analysis indicated that raw diatomite from Kenya was mainly composed of silica (SiO2), 90.73%; alumina (Al2O3), 4.51%; iron oxide (Fe2O3), 1.53%; magnesium oxide (MgO), 1.33%; calcium oxide (CaO), 0.80%; potassium oxide, (K2O), 0.69%, among other traces such as titanium (Ti), 0.14%, chlorine (Cl), 0.057% and manganese (Mn), 0.039%. The XRF studies proved that diatomite is mainly composed of silica and the results are in agreement with studies by Kipsanai (2017) and Flores-Cano et al. (2013) on diatomite from Kenya and Jalisco in Mexico respectively.

3.2 Effect of Initial Metal Ion Concentration

The effect of initial metal ion concentration on the removal efficiency of Pb (II) ions was investigated by varying the concentrations from 10mg/L to 70mg/L, while Other holding the other parameters constant (pH of 4, temperature of 25±2 oC, contact time of 60 minutes, adsorbent dose of 2g/L and shaking speed at 240rpm). Figure 2 shows the effect of initial metal ion concentration on the removal efficiency of Pb (II) ions by raw diatomite.

(a)

(b)

Figure 2: Shows the effect of initial Pb (II) ions concentration on the removal efficiency (a) and adsorption capacity (b) of raw diatomite (Contact time 60 minutes, pH of 4, adsorbent dosage 2g/L, temperature 25±2 oC, and shaking speed 240rpm).

From Figure 2, it is evident that the percentage removal of Pb (II) ions decreased with increase in initial concentration of Pb (II) ions. The removal efficiency decreased from 99.21% to 97.89% when the initial Pb (II) ion concentration was increased from 10mg/L to 70mg/L. This was due to saturation of the active sorption sites on the raw diatomite surface at higher initial concentrations. Since the adsorbent dosage used was fixed at 2g/L, it had a fixed number of active sites. Hence, at higher initial concentrations, most of the active binding sites on the adsorbent were saturated due to the presence of more Pb (II) ions compared to the available sorption sites leading lower removal efficiency. At low initial concentrations of Pb (II) ions, sufficient number of adsorption sites exists on the raw diatomite surface, therefore, more Pb (II) ions interact with the adsorbent leading to higher removal efficiency. Similar observations were observed by Sun et al. (2019) on the adsorption of lead using raw diatomite. However, the adsorption capacity of the raw diatomite for Pb (II) ions increased form 4.961mg/g to 34.264mg/g when the initial concentration was increased from 10mg/L to 70mg/L. This was attributed to the increased rate of mass transfer due to the increased diffusivity of the driving force (Gebretsadik et al., 2020).

3.3 Effect of pH

The pH value of a solution greatly influences the chemical speciation of metal ions in the sorbate and also the ionization of functional groups on the adsorbent surface (Abbar et al., 2017). The effect of pH on the adsorption of Pb (II) ions on to raw diatomite was studied by varying the pH from 2 to 6 while holding the other parameters constant. Figure 3 shows effect of pH on the removal efficiency of Pb (II) ions by the raw diatomite. It was observed that the removal efficiency increased from 77.22% to 99.21% when the solution pH was raised from 2 to 4. Further increase in pH from 4 to 6 led to a slight decrease in Pb (II) ions removal from 99.21% to 98.93%. The maximum removal efficiency was obtained at optimal pH of 4. The low removal efficiency at lower pH values was attributed to saturation of active binding sites with hydrogen ions and also due to the competition for the active binding sites between hydrogen ions and Pb (II) ions at low pH values leading to low adsorption of Pb (II)ions. In addition, the hydroxyl groups (-OH) on the diatomite surface protonate at low pH values making the diatomite surface be charge positively, therefore the positively charged surface repels the Pb (II) cations resulting in the low removal efficiency at low pH values. At higher pH values, the hydroxyl groups lose a proton making the diatomite surface to be negatively (Bilgin and Tulun, 2015, El Sayed,2018).

Figure 3: Shows the effect of pH on the removal efficiency of Pb (II) ions by raw diatomite (Contact time 60 minutes, initial Pb (II) ions concentration 10mg/L, adsorbent dosage 2g/L, temperature 25±2 oC, and shaking speed 240rpm).

3.4 Effect of Contact Time

The effect of contact time on the adsorption of Pb (II) ions onto diatomite was studied by varying the contact time from 20min to 140min at optimal initial concentrations (10mg/L) and pH (pH of 4). The adsorbent dosage, temperature and shaking speed were held constant at 2g/L, 25±2 oC and 240rpm respectively. Figure 4 shows the effect of contact time on the removal efficiency of Pb (II) ions.

Figure 4: Shows the effect of contact time on the percentage removal of Pb (II) ions by diatomite (pH of 4, initial Pb (II) ions concentration 10mg/L, adsorbent dosage 2g/L, temperature 25±2 oC, and shaking speed 240rpm).

It was observed that the Pb (II) ions removal was rapid for the first 40 minutes, then it gradually increased and equilibrium was finally reached after 60 minutes. Further increase in contact time led to no significant change in the percentage removal of Pb (II) ions. The rapid percentage removal at the beginning was due to the high number of active binding sites on the adsorbent surface. As adsorption progressed with time, these sites reduced in number leading to slow uptake of metal ions. At equilibrium, the maximum percentage removal of Pb (II) was 99.21%. El Sayed (2018) observed similar patterns for the removal of Pb (II) ions by raw diatomite from Egypt.

3.5 Effect of Temperature

The effect of temperature on the percentage removal of Pb (II) ions was investigated by varying the solution temperature from 25±2 oC to 65±2 oC while keeping the other optimal parameters constant. Figure 5 shows variations of percentage removal of Pb (II) ions with increasing temperature. From the figure, it is clear that the percentage removal of Pb (II) ions decreased slightly from 99.21% to 98.76% when the temperature was increased from 25±2 oC to 65±2 oC. The decrease in percentage removal of Pb (II) ions with increasing temperature may be due to weakening of the adsorptive forces between the Pb (II) ions and the actives sites on adsorbent surface (Thanthri et al., 2021). Hence, at higher temperatures, the rate of desorption was more significant than the rate of adsorption implying that the adsorption process was exothermic in nature (Francis, 2015). Similar trend was reported by Thanthri et al. (2021) in the adsorption of Cu2+ ions by Bael flowers. Studies by Liu et al. (2013) showed contrary behaviour in the adsorption of Pb (II) ions onto modified diatomite.

Figure 5: Shows the effect of temperature on the percentage removal of Pb (II) ions by diatomite (pH of 4, initial Pb (II) ions concentration 10mg/L, contact time 60 minutes, adsorbent dosage 2g/L, and shaking speed 240rpm).

3.6 Effect of Adsorbent Dose

The effect of adsorbent dosage on the percentage removal of Pb (II) ions was investigated by varying the adsorbent dosage from 0.4g/L to 10g/L at optimal conditions (Initial concentration 10mg/L; pH of 4; contact time of 60 minutes; temperature 25±2 oC). Figure 6 shows the percentage removal of Pb (II) ions as a function of adsorbent dosage.

Figure 6: Shows the effect of adsorbent dose on the percentage removal of Pb (II) ions by diatomite (pH of 4, initial Pb (II) ions concentration 10mg/L, contact time 60 minutes, temperature 25±2 oC, and shaking speed 240rpm).

It was observed that percentage removal of Pb (II) ions increased from 95.45% to 100% when the adsorbent dosage was increase from 0.4g/L to 4g/L. This was attributed to the increase in adsorbent surface area at higher adsorbent dosage, thereby, resulting in the availability of more binding sites for adsorption of metal ions. In addition, high adsorbent dosage led to increased probability of collision between adsorbent particles and metal ions in the solution (Dargahi et al., 2016). Similar trends were observed by Salman et al. (2016) in the removal of Pb (II) ions using diatomite from Turkey.

3.7 Adsorption isotherms

The adsorption data was applied to Langmuir, Freundlich and Temkin isotherm models in order to determine the nature of interaction between the Pb (II) ions and the adsorbent, as well as the maximum adsorption capacity. The fitting the adsorption data to these models also provides useful information on favourability of the adsorption process and adsorbate affinity for a particular adsorbent. Figures 7 represents the the Langmuir, Freundlich and Temkin isotherms isotherm for Pb (II) ions adsorption using raw diatomite. The isotherm parameters obtained are shown in table 1. The equilibrium data for the adsorption of Pb (II) ions onto raw diatomite was found to correlate well with all the isotherms but Langmuir isotherm model (R2=0.9906) agreed slightly better compared to the Freundlich (R2= 0.9846) and Temkin (R2= 0.9703) isotherm models. This indicates monolayer adsorption onto the raw diatomite surface containing a finite number of adsorption sites.

TABLE 1: Shows the Langmuir, Freundlich and Temkin isotherm parameters for the adsorption of Pb (II) ions onto raw diatomite.

| Langmuir |  |  |  |  | Freundlich |  |  |  | Temkin |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Qmax (mg/) | KL (L/m) | RL | R2 |  | Kf (L/mg) | n | R2 |  | B (J/mol) | At (L/g) | bt | R2 |
| 52.63 | 1.28 | 0.0727 | 0.9906 |  | 29.99 | 1.49 | 0.9846 |  | 10.32 | 1.43 | 240.10 | 0.9703 |

The maximum adsorption capacity for the adsorption of Pb (II) onto raw diatomite was 52.632mg/g. From the Langmuir isotherm, the separation factor value RL= 0.07272 is between 0 and 1 indicating that adsorption of Pb (II) ions onto raw diatomite is favourable. In the Freundlich isotherm model, the Freundlich constant n related to adsorption capacity has a value n=1.49. Since n>1, it indicates that the adsorption of Pb (II) ions onto raw diatomite was a physical process. In the Temkin isotherm, the parameters At and B which are equilibrium binding constant (corresponding to maximum binding energy) and parameter related to heat of adsorption were found to be 1.43 L/g and 10.32 J/mol, respectively. The positive B value (B>0) indicates the adsorption was exothermic (Batool et al., 2018; Edet and Ifelebuegu, 2020), which is in agreement with the thermodynamic study. In addition, the B value was less than 8kJ/mol (B<8kJ/mol) signifying that the adsorption of Pb (II) ions onto raw diatomite was a physical process (Nandiyanto et al., 2022; Ragadhita and Nandiyanto, 2022; Saeed-Ul-Hassan et al., 2024).

ss

(a)

(b)

(c)

Figure 7: Shows Langmuir isotherm (a), Freundlich isotherm (b) and Temkin isotherm (c) for Pb (II) ions adsorption onto raw diatomite.

3.8 Adsorption Kinetics

Adsorption kinetics describes the relationship between adsorption time and the rate of solute uptake. In this study, the adsorption kinetics of Pb (II) ions onto raw diatomite were studied for the range of contact time 0 to 140 minutes at optimal pH, initial Pb (II) ion concentration and temperature. The kinetic data obtained was applied to Lagergren’s pseudo-first-order and Ho’s pseudo-second-order kinetic models in order to describe the adsorption process. Figure 8 shows the pseudo-first-order and pseudo-second-order plots for adsorption of Pb (II) ions onto raw diatomite. The experimental and model predicted parameters obtained are tabulated in table 2. From the data, it was observed that pseudo-second order model fit well to the kinetic data with R2 =1 to describe the kinetics of adsorption of Pb (II) onto both raw diatomite compared to pseudo-first order (R2 =0.9513). This indicated that chemisorption was the rate limiting step in the sorption of Pb (II) ions onto raw diatomite. In addition, the equilibrium adsorption capacity predicted by pseudo-second order model (qe= 3.6277mg/g) was consistent with the experimental adsorption capacities (qe= 4.9605mg/g). The equilibrium adsorption capacity predicted by pseudo-first-order model (qe= 3.6277mg/g) was way different than the experimental adsorption capacity. This confirmed that pseudo-second order model was the better model to describe the adsorption of Pb (II) ions onto raw diatomite.

TABLE 2: Shows the parameters of pseudo-first order and pseudo-second order kinetic models for adsorption of Pb (II) ions

| Experimental |  | Pseudo-first-order |  |  |  | Pseudo-second-order |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| qe (mg/g) |  | qe (mg/g) | k1 (min-1) | R2 |  | qe (mg/g) | k2 (g/mg.min) | R2 |
| 4.9605 |  | 3.6277 | 0.1241 | 0.9513 |  | 4.99 | 0.2944 | 1 |

Where, k1 is the pseudo-first-order rate constant (min-1) of adsorption, qe is the adsorption capacity at equilibrium (mg/g), k2 is the rate constant of pseudo-second-order adsorption (g/mg min).

Figure 8: Shows pseudo-first-order (a) and pseudo-second-order (b) plots for the adsorption of Pb (II) ions onto raw diatomite

3.9 Adsorption Thermodynamics

Thermodynamic studies were conducted to evaluate the effect of temperature on the adsorption of Pb (II) ions onto raw diatomite. During the study, temperatures was varied (298, 308,318,328 and 338K) while keeping the other optimal parameters constant. Thermodynamic parameters namely: change in Gibbs free energy (ΔG°), enthalpy change (ΔH°) and entropy change (ΔS°) were determined in order to establish the nature of the adsorption process. The magnitude of ΔH° (kJ/mol) and ΔS° (Jmol-1K-1) were determined from the slope and intercept, respectively of the Van’t Hoff plot of lnKC against 1/T as shown in figure 9. The calculated thermodynamic parameters are shown in table 3. The Gibbs free energy (ΔG°) values obtained were all negative indicating that the adsorption processes of Pb (II) ions onto raw diatomite was feasible and spontaneous. Increase in temperature form 298K to 328K results in ΔG° values becoming more negative from -11.974 to -12.309 kJ/mol respectively, suggesting that the adsorption process became more spontaneous with increase in temperature form 298K to 328K. However, further increase in temperature from 328K to 338K led to ΔG° values becoming less negative suggesting that the adsorption of Pb (II) ions became less spontaneous at very higher temperatures. This may be due to deterioration of the raw diatomite structure at higher temperatures (above 328K) resulting in loss of adsorptive surfaces (Abunah, et al., 2019), leading to reduction in the removal efficiency of Pb (II) ions at higher temperatures.

The enthalpy change (ΔH°) value was negative, ΔH°= -8.407 kJ/mol indicating that the adsorption of Pb (II) ions onto raw diatomite was exothermic, hence increase in temperature led to decrease in the adsorption and removal efficiency. The entropy change (ΔS°) value for adsorption of Pb (II) ions onto raw diatomite was positive (ΔS°= 11.951 J/mol/K) corresponding to increase in randomness (decreased order) at the solid-solution interphase.

TABLE 3: Shows thermodynamic parameters for the adsorption of Pb (II) ions onto raw diatomite.

| ΔG° (kJ/mol) |  |  |  |  | ΔH° (kJ/mol) | ΔS° (J/mol/K) |
| --- | --- | --- | --- | --- | --- | --- |
| 298K | 308K | 318K | 328K | 338K |  |  |
| -11.974 | -12.024 | -12.204 | -12.526 | -12.309 | -8.407 | 11.951 |

Figure 9: Shows Van’t Hoff plot for adsorption of Pb (II) onto raw diatomite

4. CONCLUSION

In this work, raw diatomite from Kariandusi, Gilgil, Nakuru county, Kenya was used in the removal of Pb (II) ions from aqueous solutions. The adsorption of Pb (II) ions on to raw diatomite was greatly influenced by pH, initial Pb (II) ions concentration, contact time, adsorbent dosage and the solution temperature. Maximum percentage removal of 100% was observed at pH 4, 10mg/L initial Pb (II) ions concentration, contact time 60 minutes, adsorbent dose 4g/L and temperature 25±2 oC. The adsorption isotherm of Pb (II) ions was well described by Langmuir isotherm model. The kinetic data was well described by pseudo-second-order kinetic model (R2 =1). The thermodynamic parameters showed that the adsorption of Pb (II) ions onto raw diatomite was spontaneous and exothermic process. This study clearly shows that raw diatomite from Kenya is effective in heavy metal removal.

COMPETING INTERESTS

Authors have declared that no competing interests exist.

REFERENCES

Abbar, B., Alem, A., Marcotte, S., Pantet, A., Ahfir, N. D., Bizet, L., & Duriatti, D. (2017). Experimental investigation on removal of heavy metals (Cu2+, Pb2+, and Zn2+) from aqueous solution by flax fibres. Process Safety and Environmental Protection, 109, 639-647.

Abdelbasir, S. M., & Khalek, M. A. A. (2022). From waste to waste: iron blast furnace slag for heavy metal ions removal from aqueous system. Environmental Science and Pollution Research, 29(38), 57964-57979.

Abdulwasiu Olawale, S., Emmanuel, A., Okorie, O., Benjamen Niran, O., & Sunday Asher, A. (2022). Adsorption of Pb (II) Using Sheep Fur: Isotherm, Kinetics and Thermodynamic Studies. Asian Journal of Applied Chemistry Research, 12(4), 27-33.

Abunah, D., Onindo, C., Andala, D., & Ochoti, E. (2019). Physico-chemical removal of heavy metals from contaminated water using recyclable montmorillonite cellulose nanocomposite. Journal of Materials and Environmental Science, 10(12), 1349-1361.

Adewale, O. R., Olubunmi, O. M., Owolabi, S. A., Lawrence, O. O., Omotunde, T. O., Seun, O. T., ... & Ayemu, A. A. (2024). Kinetics, Thermodynamic and Isotherms Modeling of the Equilibrium Sorption of Pb (II), Ni (II), and Cd (II) Ions into Tiger Nut Chaff (Cyperus Esculentus) from Model Wastewater. Physical Chemistry, 13(2), 19-31.

Ajenifuja, E., Ajao, J. A., & Ajayi, E. O. B. (2017). Adsorption isotherm studies of Cu (II) and Co (II) in high concentration aqueous solutions on photocatalytically modified diatomaceous ceramic adsorbents. Applied Water Science, 7(7), 3793-3801.

Akafu, T., Chimdi, A., & Gomoro, K. (2019). Removal of fluoride from drinking water by sorption using diatomite modified with aluminum hydroxide. Journal of analytical methods in chemistry, 2019(1), 4831926.

Akinyeye, O. J., Ibigbami, T. B., & Odeja, O. (2016). Effect of chitosan powder prepared from snail shells to remove lead (II) ion and nickel (II) ion from aqueous solution and its adsorption isotherm model. American Journal of Applicated Chemistry, 4(4), 146-156.

Angon, P. B., Islam, M. S., Das, A., Anjum, N., Poudel, A., & Suchi, S. A. (2024). Sources, effects and present perspectives of heavy metals contamination: Soil, plants and human food chain. Heliyon, 10(7): 1-15

Arowojobe, Y., Aiyesanmi, A. F., & Adebayo, M. A. (2020). Removal of aqueous lead and cadmium using persea americana seed coat: single and binary studies. Advanced Journal of Chemistry-Section B, 3(1): 16-24

Ayawei, N., Ebelegi, A. N., & Wankasi, D. (2017). Modelling and interpretation of adsorption isotherms. Journal of Chemistry, 2017(1), 1-12

Azizi, B., Vaezihir, A., Siahcheshm, K., Sheydaei, M., & Aber, S. (2021). Remediation of heavy metals from contaminated river water using natural zeolite and limestone. Arabian Journal of Geosciences, 14, 1-13.

Batool, F., Akbar, J., Iqbal, S., Noreen, S., & Bukhari, S. N. A. (2018). Study of isothermal, kinetic, and thermodynamic parameters for adsorption of cadmium: an overview of linear and nonlinear approach and error analysis. Bioinorganic chemistry and applications, 2018(1), 1-11

Bilgin, M., & Tulun, Ş. (2015). Use of diatomite for the removal of lead ions from water: thermodynamics and kinetics. Biotechnology & Biotechnological Equipment, 29(4), 696-704.

Brazesh, B., Mousavi, S. M., Zarei, M., Ghaedi, M., Bahrani, S., & Hashemi, S. A. (2021). Biosorption. In  Hubbard, A. T. (Ed.). Interface Science and Technology (Vol. 33). Academic Press, London, United Kingdom. pp. 587-628.

Chaudhry, S. A., Khan, T. A., & Ali, I. (2016). Adsorptive removal of Pb (II) and Zn (II) from water onto manganese oxide-coated sand: isotherm, thermodynamic and kinetic studies. Egyptian Journal of Basic and Applied Sciences, 3(3), 287-300.

Dargahi, A., Golestanifar, H., Darvishi, P., Karami, A., Hasan, S. H., Poormohammadi, A., & Behzadnia, A. (2016). An investigation and comparison of removing heavy metals (lead and chromium) from aqueous solutions using magnesium oxide nanoparticles. Polish Journal of Environmental Studies, 25(2), 557-562.

Du, Y., Wang, L., Wang, J., Zheng, G., Wu, J., & Dai, H. (2015). Flower-, wire-, and sheet-like MnO2-deposited diatomites: Highly efficient absorbents for the removal of Cr (VI). Journal of Environmental Sciences, 29, 71-81.

Edet, U. A., & Ifelebuegu, A. O. (2020). Kinetics, isotherms, and thermodynamic modeling of the adsorption of phosphates from model wastewater using recycled brick waste. Processes, 8(6), 665-680.

El Sayed, E. E. (2018). Natural diatomite as an effective adsorbent for heavy metals in water and wastewater treatment (a batch study). Water Science, 32(1), 32-43.

Etong Inyang Daniel, John Godwin, Nasir Abdus-Salam, Aningo Nwamaka Gloria, Akor Joel Enemona, Balogun Ayo Felix, and Omale Innocent Godwin. 2025. “Synthesis, Characterization, and Application of Activated Biomaterials As Potential Adsorbents for the Removal of Cr(VI), Pb(II), and Cu(II) Ions from Aqueous Solution”. Asian Journal of Applied Chemistry Research 16 (4).133–159. https://doi.org/10.9734/ajacr/2025/v16i4363

Flores-Cano, J. V., Leyva-Ramos, R., Padilla-Ortega, E., & Mendoza-Barron, J. (2013). Adsorption of heavy metals on diatomite: mechanism and effect of operating variables. Adsorption Science & Technology, 31(2-3), 275-291.

Francis, M. M. (2015). Aluminophosphates derived from tea leaves and pumpkin seeds ashes for removal of sellected heavy metals from contaminated water (Master’s Thesis). Kenyatta University, Kenya.

Gebretsadik, H., Gebrekidan, A., & Demlie, L. (2020). Removal of heavy metals from aqueous solutions using Eucalyptus Camaldulensis: An alternate lowcost adsorbent. Cogent Chemistry, 6(1), 1720892.

Kipsanai, J. J. (2017). Exploring the use of Kenyan diatomite as a source of refractory materials. International Journal of Scientific and Research Publications, 7(10), 351-361.

Krstić, V. (2021). Role of zeolite adsorbent in water treatment. In B. A. Bhanvase, S. Sonawane, V. B. Pawade & A. B. Pandit (Eds.). Handbook of Nanomaterials for Wastewater Treatment: Fundamentals and scale up issues. Elsevier, Netherlands. pp. 417-481.

Liu, B., Luo, H., Rong, H., Zeng, X., Wu, K., Chen, Z., ... & Xu, D. (2019). Temperature-induced adsorption and desorption of phosphate on poly (acrylic acid-co-N-[3-(dimethylamino) propyl] acrylamide) hydrogels in aqueous solutions. Desalination and Water Treatment, 160, 260-267.

Liu, J., Wang, H. L., Lü, C. X., Liu, H. F., Guo, Z. X., & Kang, C. L. (2013). Remove of heavy metals (Cu2+, Pb2+, Zn2+ and Cd2+) in water through modified diatomite. Chemical Research in Chinese Universities, 29(3): 445-448.

Mishra, S. R., Chandra, R., & Kaila, J. (2017). Kinetics and isotherm studies for the adsorption of metal ions onto two soil types. Environmental Technology & Innovation, 7, 87-101.

Mustapha, S., Shuaib, D. T., Ndamitso, M. M., Etsuyankpa, M. B., Sumaila, A., Mohammed, U. M., & Nasirudeen, M. B. (2019). Adsorption isotherm, kinetic and thermodynamic studies for the removal of Pb (II), Cd (II), Zn (II) and Cu (II) ions from aqueous solutions using Albizia lebbeck pods. Applied water science, 9, 1-11.

Naik, R. L., Kumar, M. R., & Narsaiah, T. B. (2023). Removal of heavy metals (Cu & Ni) from wastewater using rice husk and orange peel as adsorbents. Materials Today: Proceedings, 72, 92-98.

Nandiyanto, A. B. D., Hofifah, S. N., Anggraeni, S., & Kurniwan, T. E. G. U. H. (2022). Isotherm adsorption of 40-μm zeolite particles for treatment of dye wastewater. Journal of Engineering Science and Technology, 17, 1265-1275.

National Environment Management Authority (NEMA). (2006). Environmental Management and Coordination, (Water Quality) Regulations 2006.

Ndung’u, S. N. (2021). Kinetic, equilibrium and thermodynamic adsorption studies of selected heavy metal ions by raw and modified jackfruit seeds from aqueous media (Masters’ Thesis). Kenyatta University, Kenya.

Ragadhita, R. I. S. T. I., & Nandiyanto, A. B. D. (2022). Curcumin adsorption on zinc imidazole framework-8 particles: Isotherm adsorption using Langmuir, Freundlich, Temkin, and Dubinin-Radushkevich models. Journal of Engineering Science and Technology, 17(2), 1078-1089.

Raji, Z., Karim, A., Karam, A., & Khalloufi, S. (2023, September). Adsorption of Heavy Metals: Mechanisms, Kinetics, and Applications of Various Adsorbents in Wastewater Remediation-A Review. Waste, 1(3), 775-805.

Saeed-Ul-Hassan, M., Ehtisham, M., Badawi, A. K., Khan, A. M., Khan, R. A., & Ismail, B. (2024). A comparative study of moisture adsorption on GO, MOF-5, and GO/MOF-5 composite for applications in atmospheric water harvesting. Nanoscale Advances, 6, 3668-3679.

Salman, T., Temel, F., Turan, N., & Ardalı, Y. (2016). Adsorption of lead (II) ions onto diatomite from aqueous solutions: Mechanism, isotherm and kinetic studies. Global NEST Journal, 18(1),1-10

Şenol, Z. M., & Şimşek, S. (2020). Removal of Pb2+ ions from aqueous medium by using chitosan-diatomite composite: equilibrium, kinetic and thermodynamic studies. Journal of the Turkish Chemical Society Section A: Chemistry, 7(1), 307-318.

Sun, L., Wang, J., Wu, J., Wang, T., Du, Y., Li, Y., & Li, H. (2019). Constructing nanostructured silicates on diatomite for Pb (II) and Cd (II) removal. Journal of Materials Science, 54(9), 6882-6894.

Thanthri, S. H. P., Ranaweera, K. H., & Perera, B. A. (2021). Adsorption study of Cu2+ ions from aqueous solutions by bael flowers (Aegle marmelos). Biointerface Res. Appl. Chem, 11(4), 11891-11904.

Tomno, R. M., Nzeve, J. K., Mailu, S. N., Shitanda, D., & Waswa, F. (2020). Heavy metal contamination of water, soil and vegetables in urban streams in Machakos municipality, Kenya. Scientific African, 9, 1-9.

Tunceli, A., Ulaş, A., Acar, O., & Türker, A. R. (2022). Adsorption isotherms, kinetic and thermodynamic studies on cadmium and lead ions from water solutions using Amberlyst 15 resin. Turkish Journal of Chemistry, 46(1), 193-205.

Uddin, M. K. (2017). A review on the adsorption of heavy metals by clay minerals, with special focus on the past decade. Chemical Engineering Journal, 308, 438-462.

Ungureanu, E. L., & Mustatea, G. (2022). Toxicity of heavy metals. In: M. H. Saleh, & I. A. Hassan (Eds.). Environmental Impact and Remediation of Heavy Metals. Intechopen Ltd, Rijeka, Croatia. pp. 18-39.

Vassileva, P. S., Apostolova, M. S., Detcheva, A. K., & Ivanova, E. H. (2013). Bulgarian natural diatomites: modification and characterization. Chemical Papers, 67(3), 342-349.

Zhang, G., Cai, D., Wang, M., Zhang, C., Zhang, J., & Wu, Z. (2013). Microstructural modification of diatomite by acid treatment, high-speed shear, and ultrasound. Microporous and Mesoporous Materials, 165: 106-112.

Zhang, P., Guo, Q., Tao, J., Ma, D., & Wang, Y. (2019). Aging mechanism of a diatomite-modified asphalt binder using Fourier-Transform Infrared (FTIR) Spectroscopy analysis. Materials, 12(6), 988-999.

Zhao, Y., Tian, G., Duan, X., Liang, X., Meng, J., & Liang, J. (2019). Environmental applications of diatomite minerals in removing heavy metals from water. Industrial & Engineering Chemistry Research, 58(27), 11638-11652.

Zulfiqar, K., Sabir, A. A., Nawaz, A. R., & Farasat, F. (2024). Urbanization in a globalized world: Reviewing environmental sustainability in developing countries. Population and Economics, 8(3), 70-85.