Original Research Article

Band-Gap Engineered TiO₂–CuO/Hydroxyapatite Photocatalyst for Efficient Treatment and Dye Degradation in Wastewater Systems

ABSTRACT

In this study, the photocatalytic degradation of methylene blue was investigated using TiO2-CuO/Hydroxyapatites Catalyst under sunlight irradiation. To enhance the photocatalytic activities of pure semiconductor photocatalysts, TiO2-CuO/Hydroxyapatites composites were successfully synthesized using the sol-gel method. The prepared composites were characterized by Fourier transform infrared spectroscopy (FT-IR), X-ray diffraction (XRD), Scanning Electron Microscopy (SEM) joined with Energy Dispersive X-ray (EDX), Thermogravimetric analysis (TGA), Brunauer, Emmett and Teller (BET) and a UV-vis diffuse reflectance spectroscopy. The results from the evaluation of the photocatalytic activity of TiO2-CuO/HAp catalyst as compared with pure HAp and TiO2 as well as CuO/HAp and TiO2/HAp composite shows an increasing order of HAp ˃ CuO/HAp ˃ TiO2/HAp ˃ TiO2-CuO/HAp in the degradation efficiencies. Hence, TiO2-CuO/HAp Composite with the least bandgap value of 2.89eV from the band gap determination of the synthesized catalysts using Tauc plot exhibited the highest degradation efficiency (99.83%) with initial methylene blue concentration of 20mg/L, dose of 0.15g and irradiation time of 150minutes under sunlight. Meanwhile, the apparent first-order rate constant (Kapp) of TiO2-CuO/HAp was 0.0430 min-1, which was higher than that of HAp, CuO, TiO2, CuO/HAp, and TiO2/HAp.The performance reusability test done on TiO2-CuO/HAp for four cycles also shows the stability of the catalyst. Finally, the application of band gap engineering techniques through the synthesis of composite materials proves TiO2-CuO/HAp is an excellent photocatalyst in the degradation of methylene blue under sunlight light irradiation.

Keywords: Bandgap, Photodegradation, TiO2-CuO/Hydroxyapatites, Methylene Blue, Reusability

1.0   INTRODUCTION

The consumption of water in many industries is almost unavoidable, especially in manufacturing industries. However, untreated effluents containing dye pollutants are discharged from many of these industries to the environment, such as the dyeing, pharmaceutical, textile, cosmetic, plastic, synthetic detergent industries, pulp, and paper, eventually leading to environmental pollution [1]. These discharged effluents from any of the above-mentioned industries contain numerous organic compounds that can cause serious human health challenges and problems for aquatic environments [1,20]. Hence, it is important to develop novel and economical methods to treat these dye pollutants. Meanwhile, several organic dye treatment methods have been reported such as thermal, physical, biological, and chemical methods [2,34]. Common among these methods is the photocatalytic degradation of dye which has been reported with relative success among researchers. The semiconductor oxides are among the most researched catalysts for this operation which can be used alone [2,3] doped [4,5] or sometimes combined with another material [6,30].

Semiconductor photocatalysts have been used for various applications which include removal of organic pollutants, CO2 reduction, water splitting, and selective synthesis of organic compounds [2,31]. Among many semiconductors is titanium dioxide (TiO2) which is an excellent photocatalyst because it’s photostable, non-toxic, inexpensive, and easily available [7]. However, due to the wide band gap (3.2 eV) of TiO2, it has become a barrier to its deployment, especially under visible light irradiation. It absorbs more ultraviolet light absorbance (<387 nm) which is 5% of the solar light than absorbing the solar light irradiation [8]. Therefore, to enhance TiO2 photoresponse to the visible light region, common among many methods of modification that have been reported are metal ion and non-metal doping [9,21], composite semiconductors formation [22], and surface dye modification by sensitization [23].

Recently, Copper oxide nanoparticles (CuO) have also attracted the attention and increasing interest of researchers because copper is one of the most important in modern technologies and because of the optical, catalytic, mechanical, and electrical properties of its nanoparticles [24]. Copper oxide (CuO) is a p-type semiconductor having a narrow bandgap of 1.2 eV and a variety of physical properties that have gained attraction in many fields such as energy conversion, magnetic, semiconductors, batteries, gas sensors, optoelectronic devices, and heterogeneous catalysis [25] and composite formation with another semiconductor oxide such as ZnO [26]. Hydroxyapatite (HAp) on the other hand has been reported to be a catalyst material of varying properties and is also studied as a catalyst support depending on its mode of synthesis which may include solid-state reaction, sol-gel method, hydrothermal technique, spray pyrolysis, microwave irradiation, hydrolysis method [27]. HAp which is usually written as Ca10(PO4)6(OH)2 belongs to the apatite family and it is a naturally occurring mineral form of Calcium apatite. It is also one of the most common forms of calcium phosphate. Thus, it is remarkably challenging to develop a novel and efficient photocatalytic material with low band gap, high chemical stability, low cost, facile synthesis, and environmental friendliness that will make it an excellent candidate for degradation of organic pollutants, CO2 reduction, water splitting under visible light irradiation [32,33].

Hence, in this study, an optimum energy gap TiO2-CuO/HAp composite was synthesized via an ‘in situ’ sol-gel method. The modified photocatalysts were characterized by several characterization tools and the bandgap of the prepared samples were determined and tuned. The photocatalytic degradation of methylene blue (MB) was used as a model reaction to evaluate the photocatalytic activities of TiO2-CuO/HAp alongside HAp, CuO, TiO2, CuO/HAp, and TiO2/HAp catalysts as control experiments. The results helped in understanding the better performance of TiO2-CuO/HAp composites as a photocatalyst. This work is innovative because it involves the synthesis of a novel metal oxide photocatalyst and engages a thorough study to evaluate the photocatalytic degradation efficiency of the TiO2-CuO/HAp catalyst in aqueous Methylene blue (MB) dye.

2.0 MATERIALS AND METHODS

2.1 Chemicals and Reagents

Titanium dioxide (TiO2) nanoparticles (purity ≥ 99.5%), Copper (II) sulfate pentahydrate   CuSO4.5H2O (purity≥99%), NaOH (purity=98%), Na2CO3 (purity = 98%), HCl (purity=95%), Acetone (purity ≥ 95%) Methylene blue (Sigma Aldrich) (purity ≥ 98%) were used for the studies. All chemicals were used in their pure form as received with no further purification.

2.2    Catalysts preparation

2.2.1 Preparation of HAp and TiO2-CuO/HAp

Hydroxylapatite was synthesized from a natural source by using bovine (cow bones) collected from the abattoir, The bones were washed with hot water and thereafter with acetone, deproteinized, dried, and carbonized at 4000C for 1 hour. The carbonized bones were milled, sieved to uniform size, and then calcined at 9000C for 2 hours. The (Ca/P) molar ratio was set at 1.67. The TiO2-CuO/HAp composite was synthesized by the sol-gel method. Briefly, 1.0g of HAp powder was dissolved in 15 ml deionized water to form a solution and stirred continuously with a magnetic stirrer. Then, 2.50g TiO2 was separately dissolved in 25 mL deionized water and stirred properly for 25 minutes at room temperature. 2.0g CuSO4·5H2O was dissolved separately also in 25 mL of deionized water and then added to the TiO2 solution and stirred continuously. Thereafter, the resulting solution was added to the HAp solution with continuous stirring at 800C for 1hr, the pH of the solution was adjusted to 10 by adding 0.25M of Sodium Carbonate (Na2CO3) solution dropwise. The dark grey precipitate formed was filtered, washed with deionized water, and dried at 800C for 4 hours. Lastly, the dried catalyst sample was subjected to 3hrs calcination time at 4000C. Similarly, for the control experiment, the synthesis of TiO2/HAp and CuO/HAp followed a similar procedure with the use of TiO2 and CuSO4·5H2O precursors respectively. Similarly, the respective precipitates formed from each synthesis were dried and calcined at 4000C for 3 hours.

2.3    Characterization

The characterization of the synthesized materials was done using various techniques. The presence of functional groups was identified by using the Fourier transform infrared (FT-IR) spectrum with a scanning range of 4000 to 1000 cm–1. For the determination of phase and crystallinity of the Hydroxylapatite (HAp) and TiO2-CuO/HAp composite, X-ray diffraction (XRD) was used, in the range, of 10°–80° at 2θ, also the surface morphologies of the materials were identified using scanning electron microscopy (SEM) joined with energy dispersive X-ray (EDX). The presence of the expected elements in the TiO2-CuO/HAp composite was ensured by the EDX spectra. Thermogravimetric analysis (TGA) was also carried out on TiO2-CuO/HAp samples. Lastly, the Brunauer, Emmett, and Teller (BET) technique was used to determine the surface area and the porosity of the synthesized TiO2-CuO/HAp catalyst.

2.4   Photocatalytic Activities Experimental Procedure

The photocatalytic degradation of methylene blue using the various catalyst samples of HAp, CuO, TiO2, CuO/HAp, TiO2/HAp, and TiO2-CuO/HAp composites was investigated under Sunlight irradiation during the sunlight period of 10:00 am and 2:00 pm. The photocatalysis of methylene blue was carried out in a 250 mL quartz beaker containing 0.15 g catalyst in 50 mL MB solution of concentration 20mg/L, pH of 9 for 150min. The pH was adjusted using HCl (0.1 M) and NaOH (0.1 M) solutions. For each experiment, the mixtures were first kept in the dark for 30 minutes with continuous stirring to attain adsorption-desorption equilibrium before it was carried out under sunlight. Finally, the comparison test and reusability of the TiO2-CuO/HAp composite were tested in four successive cycles. For each photodegradation experimental run carried out, the degradation efficiency was measured by withdrawing 5ml from the solution at regular time intervals, it was centrifuged for 10mins to remove the catalyst while the residual aliquot was analyzed by UV–Vis spectrophotometer at 664 nm wavelength. The degradation percentage was calculated by the following eq. 1.

η=Co-CtCoX 100			(1)

Where η is the degradation efficiency, Co is referred to as the initial dye concentration in solution and Ct is the concentration of dye at a specific time (t) [10].

3.0    RESULTS AND DISCUSSION

3.1     Characterization

3.1.1 Fourier Transform Infra-Red Spectroscopy.

The Fourier Transform Infrared Spectroscopy (FT-IR) analysis was used to identify the surface functional groups. FT-IR spectra of the HAp, CuO/HAp, TiO2/HAp, and TiO2-CuO/HAp are shown in Fig. 1. As shown, the characteristic peaks wave numbers of all spectra are approximately identical. The stretching modes of phosphate (PO43-) ions were detected at around 1025cm-1[11]. The stretching and broad band of OH ions hosted by the apatite were detected at around 3200-3500 cm-1 while the peak at wave number of about 120 cm-1 is attributed to the C-O from carbonate (CO32-) group in the structure [12]. The introduction of copper or Titanium into the matrix does not modify the spectrum of the Hydroxylapatite support.

Fig. 1: FTIR spectra of as-synthesized HAp-CuO/HAp catalyst

3.1.2  X-ray Diffraction (XRD) analysis

The phase analysis of the prepared HAp and TiO2-CuO/HAp catalyst was carried out by the X-ray powder diffraction (XRD) technique as shown in Fig. 2. Fig.2(a) shows the X-ray pattern with the characteristic peaks of pure HAp. The peaks were purely crystalline with hexagonal HAp phase with prominent peaks at 2θ=26.50 32-350,46.20 – 550 [13,14]. Similarly, Fig. 2(b) shows the XRD pattern of the prepared TiO2-CuO/HAp composite. The sharp peak at 2θ= 25.30, and similar peaks at 370,47.60,54.10, 63.20 indicate the formation of the anatase phase of TiO2. Further prominent peaks corresponding to 2θ=26.50, 320-350,46.20-550 are attributed to the presence of the hydroxylapatite group while the peaks at 2θ=35.50 370,48.20 signify the presence of copper ion indexed to the copper oxide in the composite.

Fig. 2(a): The XRD pattern of Hydroxyapatite (HAp)

Fig. 2(b):  The XRD patterns of TiO2-CuO/HAp composites

3.1.3   Scanning Electron Microscopy (SEM) Analysis

The surface morphology and crystal size of the derived HAp were studied under scanning electron microscopy (SEM). The SEM analysis as shown in Fig.3(a) shows an agglomeration of mixed spherical and round-shaped HAp particles with smooth surfaces likewise Fig.3(b) shows the scanning electron microscopy (SEM) image of TiO2-CuO/HAp morphology. The SEM image reveals an irregularly structured material having a flower-like surface with relatively smooth edges that is highly agglomerated into larger sizes [16].

Fig. 3(a): The SEM image of natural HAp from bovine

Fig. 3(b): The SEM image of TiO2-CuO/HAp Catalyst.

3.1.4 Energy dispersive X-ray (EDX) Analysis.

The Energy Dispersive X-ray (EDX) analysis of HAP and TiO2-CuO/HAp are presented in Figure 4(a-b). Fig. 4(a) shows the EDX spectra of natural HAp while Table 1 shows the attached elemental composition of the HAp synthesized from bovine. It was observed that the peaks of Calcium and Phosphorus are the two prominent peaks in the pattern while the percentage composition of Calcium to Phosphorus corresponds to the Ca/p ratio of 1.67 in the HAp matrix. Furthermore, the EDX analysis of TiO2-CuO/HAp with prominent peaks of the expected elements in the composites is shown in Fig. 4(b).

Fig. 4(a): The EDX analysis of natural HAp from bovine.

Table 1: Elemental Compositions of the natural HAp from Bovine.

| Element Number | Element Symbol | Element Name | Atomic Conc.(%) | Weight Conc.(%) |
| --- | --- | --- | --- | --- |
| 20 | Ca | Calcium | 67.45 | 74.26 |
| 15 | P | Phosphorus | 22.27 | 18.95 |
| 26 | Fe | Iron | 0.54 | 0.83 |
| 8 | O | Oxygen | 1.76 | 0.78 |
| 12 | Mg | Magnesium | 1.14 | 0.76 |
| 14 | Si | Silicon | 0.98 | 0.75 |
| 13 | Al | Aluminium | 0.83 | 0.62 |
| 16 | S | Sulfur | 0.68 | 0.60 |
| 7 | N | Nitrogen | 1.44 | 0.56 |
| 11 | Na | Sodium | 0.78 | 0.49 |
| 17 | Cl | Chlorine | 0.45 | 0.44 |
| 6 | C | Carbon | 1.17 | 0.39 |
| 19 | K | Potassium | 0.33 | 0.35 |
| 22 | Ti | Titanium | 0.18 | 0.24 |
| 23 | V | Vanadium | 0.00 | 0.00 |

Fig. 4(b): The EDX analysis of TiO2-CuO/HAp

3.1.5 Thermogravimetric (TGA) Analysis

The Thermogravimetric (TGA) analysis scan was recorded to study the thermal stability of the catalyst composite and to substantiate its potential in high-temperature applications. Thermo-gravimetric analysis (TGA) was carried out with a thermal analyzer and the scan is shown in Fig. 5. The scan shows a two steps weight loss pattern of the catalyst as a function of temperature between 550C and 3250C in which the weight loss of 10% percent is largely attributed to the loss of water of crystallization and further weight loss recorded was between temperature 3250C and 3800C.

Fig. 5: TGA curve for the prepared TiO2-CuO/HAp

3.1.6   Brunauer, Emmett and Teller (BET) Analysis

The Brunauer-Emmett-Teller (BET) result in Fig.6 shows that the surface area, pore volume, and pore size of the synthesized TiO2-CuO/HAp Catalyst to be 249.22(m2/g), 3.85(nm) and 0.150(cm3g-1) respectively. The result shows that the surface area of the synthesized catalyst has been enhanced with the HAp acting as the support material. Furthermore, TiO2-CuO/HAp shows an increased surface area over each of pure commercial TiO2 (98.2m2/g) [29], the nanostructured (nanotubes, nanowires, nanosheet and mesoporous) TiO2 [15] and CuO [16]. The surface area and porosity of the catalyst were investigated by the adsorption/desorption of nitrogen through the BET analysis (Fig.6). The nitrogen adsorption/desorption isotherm plot shape suggests that there is maintenance of structure and maximum adsorption capacity.

Fig. 6. The BET nitrogen adsorption-desorption isotherm plot

3.2 Optical Band Gap Estimation

The Band gap of a semiconductor material which is also known as energy gap indicates the difference in energy between the top of the valence band filled with electrons and the bottom of the conduction band lacking electrons. It is often described as the energy needed to excite an electron from the valence band to the conduction band. Therefore, the correct determination of the band gap energy is crucial in knowing the photophysical and as well as photochemical properties of semiconductors. The band gap of the prepared catalyst samples was measured with the aid of a UV-vis spectrophotometer joined with Diffuse Reflectance Spectra (DRS). The tauc plot method was used in determining the optical band gap (Eg) of the composites using the following equation:

. h.= A(h– Eg)n                                                     (2)

Where  = absorbance value is attained from the spectra, h = Planck’s constant, = c/λ, v = frequency of the incident wave, λ = wavelength from the spectra, c = velocity of light. A = constant. Eg= energy gap between the valence and conduction bands, and n = the parameter associated with the electronic transition. In this study case, indirect semiconductors n = ½. The Tauc plot showing the wavelength and the bandgaps of the synthesized materials are shown in Fig. 7 and Fig. 8(a-d) respectively. From the plot of (αhυ)1/2versus eυ, the result shows clearly that the bandgap values are 3.12eV, 3.0eV,2.92eV, 2.89eV for HAp, CuO/HAp, TiO2/HAp, TiO2-CuO/HAp respectively. Hence, this indicated that TiO2-CuO/HAp is a better photocatalyst for the photocatalytic degradation of MB under visible sunlight irradiation than the unmodified TiO2 owing to CuO being a photo-sensitizer. Furthermore, when a metal, semi-conductor catalyst, or compound is loaded to another catalyst, the previous band gap may be shifted to a new band gap [17] which may have enhanced photodegradation efficiency. Lastly, the report also shows that the band gap of the commercial CuO is 1.2eV which makes it an attractive material for light harvesting applications [18]. Therefore, in this present work, CuO is an effective bandgap modifier in the composite that helps absorb more light energy under the visible light region for effective degradation and enhanced efficiency [17,18].

Fig. 7: The UV-Vis DRS spectra of catalyst samples.

Fig. 8(a). The energy gap of HAp			        Fig. 8(b). The energy gap of CuO/HAp

Fig. 8(c). The energy gap of TiO2/HAp		     Fig. 8(d). The energy gap of TiO2-CuO/HAp

3.3    Performance and Photocatalytic Activity

The results of the photocatalytic activity of TiO2-CuO/HAp evaluated by the photodegradation of methylene blue (MB) in an aqueous solution under sunlight irradiation with MB having approximately a maximum absorption of 664nm is presented in Fig.9. TiO2-CuO/HAp photocatalytic activity was compared with the pure HAp, CuO, TiO2, CuO/HAp, and TiO2/HAp under optimum conditions and their respective photodegradation percentages were recorded in Fig.9. The result shows the least percentage degradation to be 15.52% under blank, next to this on the increasing order of photodegradetion percentages was 55.23% with pure HAp which may be associated with its higher band gap energy. Pure CuO shows 66.36% while pure TiO2 was 75.09%. Similarly, CuO/HAp shows only 79.34% MB degradation compared to TiO2/HAp (82.21%) as shown in Fig. 9. Finally, TiO2-CuO/HAp composites with the lowest band gap energy had 99.83% MB degradation, which reveals that formation of the composite improves the overall photocatalytic activity of the catalyst. This also revealed a good separation of e-/h+ pairs in TiO2-CuO/HAp composite and enhancement in surface area and active sites for efficient degradation reaction [19]. Similarly, Fig.10(a) shows the concentration ratios of methylene blue degradation using the various catalysts with maximum degradation of MB by TiO2-CuO/HAp after 150 minutes likewise Fig. 10(b) shows the apparent first-order kinetics plots of form -ln(C/C0) =kappt. The activity of the TiO2-CuO/HAp photocatalysts can be evaluated by comparing the apparent first-order rate constants (kapp) shown in Table 2. The TiO2-CuO/HAp composites have maximum apparent rate constants of 0.0430 min-1 and it decreases in the order of TiO2/HAp˃ CuO/HAp ˃ TiO2 ˃ CuO ˃ HAp progressively.

Fig. 9: Photocatalytic degradation efficiencies of MB

Fig. 10(a): The plot of 𝐶/𝐶0 versus reaction time for MB degradation

Fig. 10(b): The Plot of apparent first-order linear transforms

Table 2 : The apparent first-order rate constants (kapp) of MB degradation from the plot of -ln(C/C0) = kappt.

| Photocatalyst | -ln(C/C0)=kappt | kapp (min-1) |
| --- | --- | --- |
| HAp | -ln(C/C0)=0.0094t | 0.0094 |
| CuO | -ln(C/C0)=0.0142t | 0.0142 |
| TiO2-CuO/HAp | -ln(C/C0)=0.0430t | 0.0430 |
| TiO2 | -ln(C/C0)= 0.0182t | 0.0182 |
| TiO2/HAp | -ln(C/C0)= 0.0346t | 0.0346 |
| CuO/HAp | -ln(C/C0)= 0.0226t | 0.0226 |

3.4    Reusability Study of the Catalyst

The stability and reusability of the prepared TiO2-CuO/HAp catalyst were assessed by recycling the catalyst for four successive runs for the degradation of methylene blue as shown in Fig. 11. In each experimental cycle, the catalyst was separated from its suspension by centrifugation and then washed with deionized water before it was finally dried. The degradation efficiency of the MB was evaluated and the result shows that 99.53% efficiency was achieved in the first run while 95.32% in the second run, 91.15% was recorded in the third run, and 87.67% during the fourth cycle with each experiment carried out under sunlight light irradiation for 150 minutes. The slight decrease in the subsequent photocatalytic activity may be attributed to a small amount of metal ions leached from the catalyst surface or some intermediates adsorb on the surface of the catalyst [20]. Nevertheless, the degradation efficiency was relatively close for the four runs which demonstrates that the catalytic performance of TiO2-CuO/HAp may be replicated in successive runs without much significant drop in the efficiency.

Fig.11:The photocatalytic degradation rate of MB with the TiO2-CuO/HAp catalyst at different
recycling times.

3.5 Possible Photocatalytic Mechanism

A possible photocatalytic mechanism of the TiO2-CuO/HAp composite is shown in Fig.12. TiO2 is an n-type semiconductor and the band gap between the valance band (VB) and the conduction band (CB) is 3.2 eV while that of CuO is 1.2eV [28]. Under light irradiation, electrons, and holes are generated on the surface of TiO2 and CuO. The electrons in the CB of TiO2 are easily transferred to the CB of CuO because the CB of CuO is located below that of TiO2. On the other hand, through the anchoring of TiO2 and CuO on the Hydroxylapatite (HAp) support, the photoelectrons of TiO2 and CuO are enhanced via improved active sites for reaction which in turn may lower the electron-hole recombination rate. Results show that TiO2-CuO/HAp composite can exhibit an effective electron-hole separation under solar irradiation and consequently facilitate the surface redox process via the photogenerated electrons and holes. Hence, a significant improvement in the photocatalytic activity of the catalyst. The electron–hole pair generation under sunlight light irradiation inside the CB and VB helps in the degradation of dye molecules (MB) with the generation of water molecules (H2O) and carbon dioxide (CO2) as by-products.

Fig.12. The photocatalytic mechanism of the TiO2-CuO/HAp composite.

4.0   CONCLUSIONS

TiO2-CuO/HAp catalyst was synthesized via the sol-gel method and characterized by the following techniques: FT-IR, XRD, SEM, EDX, TGA, and BET. The analysis indicates that the samples were composed of HAp, TiO2, and CuO nanoparticles. The experiments on photocatalytic degradation of methylene blue showed that the TiO2-CuO/HAp exhibited higher degradation percentage and MB absorption as compared to HAp, CuO, TiO2, CuO/HAp, and TiO2/HAp composites with high apparent first-order rate constant (kapp) of 0.0430min-1. The bandgap of the synthesized TiO2-CuO/HAp was determined to be 2.89eV. Hence, through the band gap engineering technique, the wide band gap of TiO2 can be modified to facilitate its operation within the visible light range. This suggests that methylene blue can be degraded with the catalyst efficiently with the use of sunlight Irradiation. Therefore, the use of sunlight may be a promising process for reducing operating costs as compared to the use of artificial visible light.

AVAILABILITY OF DATA AND MATERIALS

The research data associated with this paper will be made available upon request.

DISCLAIMER (ARTIFICIAL INTELLIGENCE)

Author(s) hereby declare that NO generative AI technologies such as Large Language Models  (ChatGPT, COPILOT, etc.) and text-to-image generators, have been used during the writing or  editing of this manuscript.

REFERENCES

[1] Thuan, D.V., Ngo, H. L., Thi, H. P., Chu, H. T. (2023). Photodegradation of hazardous organic pollutants using titanium oxides-based photocatalytic: A review. Environmental Research, 229, 116000 https://doi.org/10.1016/j.envres.2023.116000

[2] Singh, N. K., Saha, S., Pal, A. (2014). Methyl red degradation under ultra-violet illumination and catalytic action of commercial ZnO: A parametric study. Desalination and Water Treatment, 56,1–11. https://doi.org/10.1080/19443994.2014.942380

[3] Yu, J., Yu, X. (2008). Hydrothermal synthesis and photocatalytic activity of zinc oxide hollow spheres, Environ. Sci. Technol., 42 (13), 4902–4907. DOI: 10.1021/es800036n

[4] Wang, M., Huang, C., Huang, Z., Guo, W., Huang, J., He, H., Wang, H., Cao, Y., Liu, Q., Liang, J. (2009). Synthesis and photo-luminescence of Eu-doped ZnO microrods prepared by hydrothermal method, Optical Material, 31 (10), 1502–1505. https://doi.org/10.1016/j.optmat.2009.02.009

[5] Zhang, X., Liu, Y., Ren, M., Yang, G., Qin, L., Guo, Y., Meng, J. (2022). Precise carbon doping regulation of porous graphitic carbon nitride nanosheets enables elevated photo-catalytic oxidation performance towards emerging organic pollutants. Chem. Eng. J., 433, https://doi.org/10.1016/J.CEJ.2022.134551 134551.

[6] Chen, T., Zheng, Y., Lin, J.-M., Chen, G. (2008). Study on the photocatalytic degradation of methyl orange in water using Ag/ZnO as a catalyst by liquid chromatography-electrospray ionization ion-trap mass spectrometry, J. Am. Soc. Mass Spectrom., 19 (7), 997–1003

[7] Lu, D., Zhang, G. K. & Wan, Z. (2015). Visible-light-driven g-C3N4/Ti3+-TiO2 photocatalyst co-exposed {001} and {101} facets and its enhanced photocatalytic activities for organic pollutant degradation and Cr(VI) reduction. Appl. Surf. Sci., 358, 223–230. https://doi.org/10.1016/j.apsusc.2015.08.240

[8] Low, J. X., Cheng, B. & Yu, J. G. (2017). Surface modification and enhanced photo-catalytic CO2 reduction performance of TiO2: a review. Appl. Surf. Sci., 392, 658–686. https://doi.org/10.1016/j.apsusc.2016.09.093

[9] Wen, J. Q., Li, X., Liu, W., Fang, Y., Xie, J., Xu, Y. (2015). Photocatalysis fundamentals and surface modification of TiO2 nanomaterials. Chinese. J. Catal., 36, 2049–2070 (2015). https://doi.org/10.1016/S1872-2067(15)60999-8

[10] Saravanan, R.  Sacari, E.  Gracia, F. Khan, M.M., Mosquera, E., Gupta, V.K. (2016). Conducting PANI stimulated ZnO system for visible light photocatalytic degradation of color dyes, J. Mol. Liquids, 221, 1029–1033. https://doi.org/10.1016/j.molliq.2016.06.074

[11] Ning, Z.L., Chang, Z.D., Li, W.J., Sun, C.Y., Zhang, J.H., Liu, Y. (2012). Solvothermal synthesis and optical performance of one-dimensional strontium hydroxyapatite nanorod, J. Chem. Eng., 20, 89–94 https://doi.org/10.1016/S1004-9541(12)60367-X

[12] Landi, E., Celotti, G., Logroscino, G., Tampieri, A. (2003). Carbonated hydroxyapatite as a bone substitute, J. Eur. Ceram. Soc. 23, 2931–2937. https://doi.org/10.1016/S0955-2219(03)00304-2

[13] Padmanabhan, P. V., Kulandaivelu, R., Panneer, D.S., Vivekananthan, S., Sagadevan, S. & Lett., J. A. (2019). Microwave synthesis of hydroxyapatite encumbered with ascorbic acid intended for drug leaching studies, Materials Research Innovations, 1-7. DOI:10.1080/14328917.2019.1624940

[14] Manalu, J. L., Soegijono, B., Indrani, D. J. (2015). Characterization of Hydroxyapatite Derived from Bovine Bone. Asian Journal of Applied Sciences, 03(4), 758-765, www.ajouronline.com.

[15] Sasaki, T., Nakano, S., Yamauchi, S. and Watanabe, M. (1997). Fabrication of titanium dioxide thin flakes and their porous aggregate, Chem. Mater., 9, pp. 602-608. DOI:10.1021/cm9604322

[16] Xu, L., Xu, H-Y., Wang, F., Zhang, F-J., Meng, Z-D., Zhao, W., and Oh, W-C. (2012). Microwave-Assisted Synthesis of Flower-like and Plate-like CuO Nanopowder and their photocatalytic activity for polluted lake water, Journal of the Korean Ceramic Society, 49(2), pp 151-154.

http://dx.doi.org/10.4191/kcers.2012.49.2.151

[17] Karim, K.R., Jebi, M.P., Ong, H.R., Abdullah, H., Tarek, M., Cheng, C. K., Khan. M.R. (2018). CuO-TiO2 as a visible light responsive photocatalyst for the photo- electroreduction of CO2 to methanol, Conference Paper December, 103-111.https://www.researchgate.net/publication/329876632

[18] Dhineshbabu, N. R., Rajendran, V., Nithyavathy, N., Vetumperumal. R. (2016). Study of structural and optical properties of cupric oxide nanoparticles, Appl. Nanosci., 6:933–939.

doi:10.1007/s13204-015-0499-2

[19] Alafif, Z.A., Anjum, M., Kumar, R., Abdelbasir, S.M., Barakat, S.A. (2018). Synthesis of CuO–GO/TiO2 visible light photocatalyst for 2 chlorophenol degradation, pretreatment of dairy wastewater, and aerobic digestion. J. of Appl. Nanosci., 1-13, doi.org/10.1007/s13204-018-0921-7.

[20] Ahmed, Y. Y., Yaakob, Z., and Akhtar, P. (2016). Degradation and mineralization of methylene blue using a heterogeneous photofenton catalyst under visible and solar light irradiation. The Royal Society of Chemistry, Catalysis Science and Technology, 6, 1222-1232, doi: 10.1039/c5cy01494h.

[21] Yang, Y. F., Ma, Z., Xu, L., Wang, H., Fu, N. (2016) Preparation of reduced graphene oxide/meso-TiO2/AuNPs ternary composites and their visible-light-induce photocatalytic degradation of methylene blue. Appl. Surf. Sci., 369, 576–583, https://doi.org/10.1016/j.apsusc.2016.02.078

[22] Li, Y. F., Zhang, W., Shen, X., Peng, P., Xiong, L., Yu, Y. (2015). Octahedral Cu2O-modified TiO2 nanotube arrays for efficient photocatalytic reduction of CO2. Chinese. J. Catal., 36, 2229-2236

https://doi.org/10.1016/S1872-2067(15)60991-3

[23] Qi, K. Z., Selvaraj, R., Al-Fahdi, T., Al-Kindy, S., Kim, Y., Wang, G. C., Tai, C. W., Sillanpaa, M. (2016). Enhanced photocatalytic activity of anatase-TiO2 nanoparticles by fullerene modification: A theoretical and experimental study. Appl. Surf. Sci., 387,750–758. https://doi.org/10.1016/j.apsusc.2016.06.134

[24] Singh, J., Kaur, G. and Rawat, M. (2016). A brief review on synthesis and characterization of copper oxide nanoparticles and its applications. Journal of Bioelectronics and Nanotechnology, 1(1): 9, DOI: 10.13188/2475-224X.1000003

[25] Darezereshki, E. and Bakhtiari, F. (2011). A novel technique in the synthesis of tenorite (CuO) nanoparticles from low concentratIon cuso4 Solution. J. Min. Metall. Sect. B-Metall.,  47 (1) B, 73 - 78

[26] Widiarti, N., Sae, J. K. and Wahyuni, S. (2017). Synthesis of CuO-ZnO nanocomposite and its

application as an antibacterial agent. Materials Science and Engineering, 172, 012-036,

doi:10.1088/1757-899X/172/1/012036

[27] Linh, T.-T, Hong, S., and No, K. (2019). Evaluation of the Role of Hydroxyapatite in TiO2/Hydroxyapatite Photocatalytic Materials. J. of Intech.Open., 1-11, http://dx.doi.org/10.5772/intechopen.81092.

[28] Etape, E.P., Ngolui, L.J., Foba-Tendo, J., Yufanyi, D.M. and Namondo, B.V. (2017). Synthesis and characterization of CuO, TiO2, and CuO-TiO2 mixed characterization of CuO, TiO2, and CuO-TiO2 mixed Oxide by a modified oxalate route. Journal of Applied Chemistry, 7,2017, 1-10. https://doi.org/10.1155/2017/4518654

[29] Drunka, R., Grabis, J., Krumina, A. (2016). Microwave Assisted Synthesis, Modification with Platinum, and Photocatalytic Properties of TiO2 Nanofibers, 22(1),138-141.

http://dx.doi.org/10.5755/j01.ms.22.1.7353

[30] Zhao, G., Li, W., Zhang, H., Wang, W., Ren, Y. (2022). Single-atom Fe-dispersed graphitic carbon nitride (g-C3N4) as a highly efficient peroxy-mono sulfate photocatalytic activator for sulfamethoxazole
degradation. Chem. Eng. J., 430, https://doi.org/10.1016/J.CEJ.2021.132937 132937

[31] Zhao, B., Gao, D., Liu, Y., Fan, J., Yu, H. (2022). Cyano-group enriched crystalline graphitic carbon nitride photocatalyst: Ethyl acetate-induced improved ordered structure and efficient hydrogen evolution activity. J. Colloid Interface Sci. 608, 1268–1277.  https:// doi.org/10.1016/J.JCIS.2021.10.108

[32] Zhang, J., Fu, J., Dai, K. (2022). Graphitic carbon nitride/antimonide van der Waals heterostructure with enhanced photocatalytic CO2 reduction activity. J. Mater. Sci. Technol. 116, 192–198. https://doi.org/10.1016/J.JMST.2021.10.045

[33] Cheng, L., Zhang, P., Wen, Q., Fan, J., Xiang, Q. (2022). Copper and platinum dual single atoms supported on crystalline graphitic carbon nitride for enhanced photocatalytic CO2 reduction. Chinese J. Catal., 43, 451–460. https://doi.org/10.1016/S1872-2067(21) 63879-2.

[34] Oladoye, P.O., Kadhom, M., Khan, I., Hama Aziz, K. H., Alli, Y. A. (2024). Advancements in adsorption and photo-degradation technologies for rhodamine B dye wastewater treatment: Fundamentals, applications, and future directions. Journal of Green Chemical Engineering, 5(4), 440-460. https://doi.org/10.1016/j.gce.2023.12.004