Original Research Article

Enhancing Natural Dye Affinity on Wool Through Optimized ZnO Nanoparticle Mordanting

ABSTRACT

Background: Nowadays, there is an increasing awareness among consumers towards the use of natural dyed textiles. Natural dyes have better biodegradability and generally have high compatibility with the environment. Most of the natural dyes are non-substantive dyes and therefore need a mordant to help them bond with fibres. The use of nano materials, an alternative to metal-based mordants, is attracting attention of researchers to improve colour and functional properties of treated dyed textiles. However, limited research exists on the effectiveness of inorganic nanoparticles as sustainable mordants in natural dyeing, particularly with kachnar dye on wool. Thus, focusing on the benefits of natural dyes, wool fabric was dyed with kachnar dye in presence of inorganic nanoparticles as mordants.

Methods: To achieve the objectives of study, four different inorganic nanoparticles were explored to ascertain the effect of nano treatment on dye uptake and colour fastness of wool fabric. Neutral scouring of wool fabric was done to improve its absorbency. The scoured wool fabric was treated separately with nanoparticles and simultaneously dyed with kachnar dye. On the basis of maximum dye absorption (%), colour strength (K/S) and wash fastness (CC and CS) grades, one nanoparticle was selected. Nano treatments for wool fabric were optimized for different process parameters viz. treatment stage, nanoparticle concentration, treatment pH, time, temperature and M:L ratio of treatment bath on the basis of maximum dye absorption (%) and colour properties of treated dyed wool fabric.

Results: On the basis of colour strength and colour properties of treated dyed wool fabric samples, one nanoparticle i.e. zinc oxide was selected for natural dyeing of wool fabric with kachnar dye. The optimized conditions and concentrations for nano treatment and dyeing of wool fabric were simultaneous stage of treatment, 1.00 % conc. of zinc oxide nanoparticle, 40 minutes treatment duration with 80℃ temperature, 5.5 pH value and 1:40 M:L ratio.

Conclusions: The study highlights the potential of nanoparticle-assisted natural dyeing as a more sustainable alternative to conventional metal mordants, which often pose environmental and wastewater-treatment concerns. Among the four nanoparticles tested, zinc oxide proved to be the most effective in improving dye uptake, colour strength and wash fastness. By reducing reliance on heavy metals and improving process efficiency, ZnO nanoparticles offer a promising eco-friendly approach for natural dyeing of wool fabric.

Key words: Wool, Natural dye, Nanoparticles, Eco-friendly, Colour properties

1. INTRODUCTION

In recent years, the global textile industry has experienced a significant shift toward sustainable and environmentally responsible production methods. Growing concerns over climate change, environmental pollution and resource depletion have intensified the search for greener alternatives to conventional textile chemicals (Jiang et al., 2022). Among these, synthetic dyes have attracted particular scrutiny due to their toxic by-products, high chemical oxygen demand (COD) and the persistence of residues in aquatic ecosystems. Wastewater from dyeing operations often contains carcinogenic and mutagenic compounds that pose long-term environmental and health risks. As a result, the development of eco-friendly dyeing practices has become a priority for both researchers and industry stakeholders (Haijuan et al., 2022; Rani et al., 2025).

Natural dyes, derived from plant, animal and mineral sources, provide a renewable and biodegradable alternative to synthetic dyes. Their low toxicity, minimal environmental impact and potential for value addition to agricultural by-products have contributed to a renewed scientific interest in their application to textile fibres (Memon et al., 2016). However, despite their ecological advantages, natural dyes often suffer from limitations such as lower dye uptake, inadequate fastness properties and limited shade ranges. Overcoming these drawbacks is crucial to making natural dyeing a viable industrial alternative (Singh and Jahan, 2019; Kiakhani et al., 2019).

Kachnar (Bauhinia variegata), a deciduous tree is known for its vibrant pink and purple flowers. These flowers contain flavonoids, anthocyanins and tannins, bioactive compounds capable of producing rich and aesthetically pleasing shades on natural fibres such as wool. Utilizing Kachnar as a dye source not only promotes the use of locally available and renewable plant materials but also adds value to a botanical resource traditionally used in herbal and culinary applications. Despite its promising dyeing potential, Kachnar dye exhibits challenges typical of many plant-based dyes, such as limited fibre affinity and inadequate colour fastness, especially when applied without a mordant (Barani et al., 2017; Ashique et al., 2025).

Mordants play a critical role in natural dyeing by forming coordination bonds between dye molecules and fibre surfaces, thereby improving colour depth and fastness. Conventional mordants such as alum, iron and copper salts have been widely used, yet their environmental impact and limited functional enhancement have prompted the exploration of more advanced alternatives. In this context, nanotechnology offers a novel and increasingly popular approach for addressing the shortcomings of natural dyes (Rahman et al., 2022).

Inorganic nanoparticles have demonstrated significant potential in textile finishing and coloration. Their nanoscale dimensions provide a large surface-to-volume ratio, enabling enhanced interactions with dye molecules and fibre substrates. When used as nanoparticle mordants, these materials can improve dye adsorption, increase surface roughness, promote deeper penetration of dye molecules and impart additional functional properties such as antimicrobial activity, UV protection and improved wash durability. Moreover, nanoparticles can facilitate the formation of stronger and more stable bonds between natural dyes and wool keratin, thus contributing to better overall colour performance (Rastogi and Aggarwal, 2017; Rather et al., 2024).

Wool, a natural protein fibre, possesses distinct chemical and physical characteristics that make it compatible with natural dyes. The presence of amino, carboxyl and hydroxyl groups in wool’s molecular structure enables effective bonding with natural dye molecules, especially when assisted by mordants. The integration of nanoparticles into the dyeing process may further enhance these interactions and reduce reliance on environmentally harmful chemical mordants (Pandey et al., 2018). Given this background, the present study aims to investigate the eco-friendly dyeing of wool fabric using kachnar dye in combination with selected inorganic nanoparticles.

2. MATERIALS AND METHODS

2.1 Procurement of fabric: Samples of pure greige woven wool fabrics of medium weight were collected from market of Hisar. Purity of collected samples were examined by burning, microscopic and chemical tests. Based on visual inspection and fabric composition, the wool fabric suitable for apparel purpose was chosen for further work.

2.2 Preparation of wool fabric for dyeing: “The selected wool fabric was initially weighted and pre-wetted in plain water for 10-15 minutes. It was then entered into scouring bath containing required amount of neutral detergent (2 g/l) keeping material to liquor ratio 1:20 and pH 7:0. The temperature of the bath was gradually raised to 60oC and fabric was treated for 60 minutes with intermittent stirring. The scoured fabric was then rinsed with plain water and dried at ambient temperature” (Rukhaya, 2020).

2.3 Determination of preliminary properties of wool fabric: The preliminary data of wool fabric was taken under three parameters i.e. fabric count, weight and thickness using standard test methods. Pick glass with pointer was used to determine the fabric count of the wool fabric using ASTM-D123 test method. The weight of one square meter of the fabric was calculated as per ASTM-D3776-90 test method by multiplying the weight of specimen in grams with 100. Digital thickness tester was used to measure thickness of the fabrics using ASTM-D 1777-60 test method.

2.4 Procurement of dye material: The dye material i.e. kachnar bark was procured from market of Hisar. The bark was dried in shade and crushed into small pieces, grounded into fine powder. The prepared dye powder was stored in the air tight containers to keep them free from environmental influences, till usage.

2.5 Preparation of dye extract:  The 6 g dye powder was soaked in 50 ml distilled water for 24 hours. Aqueous extract of kachnar bark dye was prepared by boiling the soaked dye solution for 20 minutes and filtered to obtain first filterate. The percolation was repeated twice to obtain the second and third filterate. All the three dye filtrates were mixed thoroughly and the dye solution so obtained was used for dyeing of fabric samples.

2.6 Phytochemical analysis of kachnar bark dye extract: The active chemical components of kachnar bark dye i.e. flavonoids, glycosides, phenol, saponins, tannins and terpenoids present in the dye were identified using standard procedures.

2.7 Procurement and selection of nanoparticles for dyeing of wool fabric: Four different inorganic nanoparticles i.e. Aluminium oxide (Al2O3., 70nm), Copper oxide (CuO, 80nm), Titanium dioxide (TiO2, 75 nm) and Zinc oxide (ZnO, 65 nm) were tried as mordants. All the nanoparticles were procured from Central Drug House (P) Ltd., New Delhi, India. All the four nanoparticles were applied separately on the scoured wool fabric and one nanoparticle was selected on the basis of maximum per cent dye absorption, colour strength (K/S) and wash fastness in terms of colour change (CC) and colour staining (CS) of dyed wool fabric samples.

2.8 Standardization of nanoparticle treatment for dyeing of wool fabric: Six process variables i.e. nanoparticle treatment stage, nanoparticle concentration, treatment pH, treatment time, treatment temperature and material-to-liquor ratio (MLR) were optimized based on percent dye absorption, colour strength (K/S) and wash fastness (CC and CS) of the nanoparticle treated dyed samples. For optimization, scoured wool fabric was subjected to various levels of each treatment variable. After nanoparticle treatment, the samples were allowed to cool to room temperature in the treatment bath, then squeezed and immediately dyed with kachnar dye.

Both untreated and nanoparticle treated wool samples were dyed for 60 minutes at 90°C using a material-to-liquor ratio of 1:20 in an Infrared (IR) Beaker Dyeing Machine. Following dyeing, the samples were rinsed and then soaped with 2 g/L Ultravon JU solution at 60°C, maintaining a M:L ratio of 1:20 for 15-20 minutes. Finally, the dyed fabrics were thoroughly washed with cold water, squeezed and air-dried at room temperature.

3. RESULTS AND DISCUSSION:

3.1 Preliminary properties of wool fabric: The wool fabric was scoured to remove all the impurities and fabric count, weight and thickness of the resultant fabric were measured. The data presented in Table 1 depict that fabric count of greige wool fabric in warp and weft direction was 55×45 ends and picks per inch with fabric weight 162.20 g/m2 and thickness 0.372 mm whereas the fabric count of scoured wool fabric was 59×49 ends and picks per inch with fabric weight 153.40 g/m2 having 0.462 mm thickness.

The fabric count of scoured fabric increased in warp and weft directions by 6.77 and 8.16 per cent respectively and fabric weight decreased by 5.55 per cent. Thickness of scoured fabric increased by 24.19 per cent as compared with the greige fabric.

Table 1: Preliminary properties of wool fabric

| Samples | Fabric count (ends and picks/inch) |  |  |  |  | Fabric weight (g/m2) |  | Fabric thickness (mm) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Warp mean ± SE (m) | Per cent change | Weft mean ± SE (m) | Per cent change | Mean (warp+weft) | Mean ± SE (m) | Per cent change | Mean ± SE (m) | Per cent change |
| Greige | 55±0.447 | - | 45±0.400 | - | 54.0 | 162.20±0.374 | - | 0.372±0.003 | - |
| Scoured | 59±0.447 | +6.77 | 49±0.583 | +8.16 | 50.0 | 153.40±0.400 | -5.55 | 0.462±0.003 | +24.19 |

SE = Standard error; + Increase in property; - Decrease in property,

Hence, it is inferred that after scouring fabric count and weight of the greige wool fabric decreased while the fabric thickness was found to be increased. Anita, 2020 also noticed that fabric count and weight decreased after scouring of wool fabric with neutral detergent and the thickness was observed to be increased.

3.2 Phytochemical analysis of kachnar dye extract: Extraction of kachnar dye was done in aqueous medium and qualitative phytochemical analysis of extract was conducted for identification of the active substances in kachnar dye.

Kachnar Bark

Dye Powder

Dye Extract

Plate 1: Kachnar Dye

Table 2: Phytochemical analysis of kachnar dye

| Sr. No. | Phytochemicals | Kachnar dye |
| --- | --- | --- |
| 1. | Flavonoids | - |
| 2. | Glycosides | + |
| 3. | Phenol | + |
| 4. | Saponins | + |
| 5. | Tannins | + |
| 6. | Terpenoids | + |

Table 2 indicates that phytochemical analysis of kachnar dye exhibited the presence of glycosides, phenol, saponins, tannins and terpenoids in considerable quantity whereas flavonoid is not present in kachnar dye. The findings are in line with Sharma, 2019 that phytochemical analysis of kachnar bark dye demonstrated the presence of glycosides, phenols, saponins, tannins and terpenoid while the absence of flavonoid.

3.3 Selection of nanoparticles for treatment of wool fabric: The data in Table 3 depict that the untreated wool fabric samples dyed with kachnar bark exhibited 19.13 per cent dye absorption having 14.84 colour strength with good (4) and fairly good (3/4) wash fastness grades in terms of colour change and colour staining respectively. When dyeing of wool fabric was done with kachnar bark in presence of aluminium oxide nanoparticles, the per cent dye absorption (26.15%), colour strength (18.02) and wash fastness grades for colour change (4, good) and colour staining (4/5, very good) were recorded to be elevated as compared to untreated dyed wool fabric. Similarly, nano copper oxide treated wool fabric samples dyed with kachnar dye had improved per cent dye absorption (26.78%), colour strength (18.74) with and good (4) washing fastness grades for change in colour very good (4/5) for colour staining in comparison to untreated dyed wool fabric sample.

Table 3: Selection of nanoparticles for treatment of wool fabric

| Treated dyed samples | Per cent dye absorption | Colour strength (K/S) | Wash fastness grades |  |
| --- | --- | --- | --- | --- |
|  |  |  | (CC) | (CS) |
| Untreated (Control) | 19.13 | 14.84 | 4 | 3/4 |
| Nano aluminium oxide | 26.15 | 18.02 | 4 | 4/5 |
| Nano copper oxide | 26.78 | 18.74 | 4/5 | 4 |
| Nano titanium dioxide | 25.95 | 17.45 | 4 | 4/5 |
| Nano zinc oxide | 27.78 | 19.44 | 5 | 4/5 |

CC: Colour change; CS: Colour staining

The data in Table 3 further reveal that the treatment of wool fabric with titanium dioxide nanoparticles enhanced the per cent dye absorption (25.95%), colour strength (17.45) and wash fastness grades for change in colour (4, good) and colour staining (4/5, very good). When treatment with zinc oxide nanoparticles and dyeing of wool fabric with kachnar bark was carried out, the per cent dye absorption was 27.78 per cent, colour strength was 19.44 and washing fastness grades for change in colour and colour staining were excellent (5) and very good (4/5) respectively.

It was envisaged that amongst all the nanoparticles treated kachnar bark dyed wool fabric samples, nano zinc oxide treated wool fabric dyed with kachnar bark dye exhibited highest per cent dye absorption (27.78 %), maximum colour strength (19.44) with excellent wash fastness grades towards change in colour (5) and very good (4/5) wash fastness rating to colour staining. Therefore, nanoparticles of zinc oxide were selected for treatment of wool fabric while dyeing with kachnar bark dye. According to Montazer and Seifollahzadeh (2011) metallic nanoparticles of TiO2, Al2O3, ZnO, CuO, Fe2O3 and MgO are being widely used for colouration of textiles as well as imparting antimicrobial, UV protection and antistatic finish because of their photocatalytic ability. The results of the present study are in agreement with Bhandari (2021) that nano copper oxide, iron oxide and zinc oxide displayed maximum percent dye absorption, colour strength and wash fastness ratings with natural dyes on wool fabric. Tangkawanit and Keawsri (2023) found that ZnO NPs coated and indigo dyed silk fabric samples exhibited excellent washing fastness properties.

Untreated Dyed (Control)

Nano Copper Oxide Treated Dyed

Nano Aluminium Oxide Treated Dyed

Nano Zinc Oxide Treated Dyed

Nano Titanium Dioxide Treated Dyed

Plate 2: Shades Obtained with Kachnar Bark Dye on Nanotreated Wool Fabrics

3.4 Standardization of nanoparticle treatment for wool fabric: To enhance the dyeing efficiency and colour properties of wool fabric with kachnar dye, the variables of nanoparticle treatment with zinc oxide (ZnO) were optimized.

i. Optimization of nanoparticle treatment stage: The results related to optimization of nanoparticle treatment stage are presented in Table 4.

Table 4: Optimization of nanoparticle treatment stage on basis of dye absorption and colour properties of dyed wool fabric

| Treatment stage | Nanoparticle treated dyed samples |  |  |  |
| --- | --- | --- | --- | --- |
|  | Per cent dye absorption | Colour strength (K/S) | Wash fastness grades |  |
|  |  |  | (CC) | (CS) |
| Pre treatment | 24.64 | 15.77 | 4 | 4 |
| Simultaneous treatment | 27.78 | 19.44 | 5 | 4/5 |
| Post treatment | 25.08 | 16.18 | 4/5 | 4/5 |

CC: Colour change; CS: Colour staining

It is clear from the table that when dyeing of wool fabric with kachnar dye was carried out in the presence of zinc oxide nanoparticles, the highest per cent dye absorption (27.78%) was observed at simultaneous stage of nanoparticle treatment with highest colour strength (19.44) value and excellent (5) wash fastness grade for colour change and very good (4/5) wash fastness grade for colour staining. The application of zinc oxide nanoparticles at pre and post stages reflected 24.64 and 25.08 per cent dye absorption with 15.77 and 16.18 colour strength values and good (4) to very good (4/5) wash fastness towards colour change and colour staining respectively.

Hence, on the basis of maximum per cent dye absorption and colour properties, simultaneous treatment stage was selected as optimum nanoparticle treatment stage for application of zinc oxide nanoparticles when dyeing with kachnar dye. Moulik et al. (2021) used the aqueous extract of eucalyptus bark for simultaneous dyeing of cotton, silk, wool and eri silk fabrics in the presence of metallic mordants. Haijuan et al. (2022) supported the findings that addition of ZnO nanoparticles as mordant during dyeing greatly increased the dye exhaustion and enhanced the colour strength of treated dyed silk fabric.

ii. Optimization of nanoparticle concentration: The results regarding optimization of nanoparticle concentration are incorporated in Table 5.

Table 5: Optimization of nanoparticle concentration on the basis of dye absorption   and colour properties of dyed wool fabric

| Concentrations (%) | Nanoparticle treated dyed samples |  |  |  |
| --- | --- | --- | --- | --- |
|  | Per cent dye absorption | Colour strength (K/S) | Wash fastness grades |  |
|  |  |  | (CC) | (CS) |
| 0.25 | 21.32 | 16.32 | 3/4 | 4 |
| 0.50 | 23.96 | 17.58 | 4 | 4/5 |
| 0.75 | 23.75 | 15.12 | 4 | 4 |
| 1.00 | 27.78 | 19.44 | 5 | 4/5 |
| 1.25 | 27.13 | 18.45 | 4/5 | 4/5 |

CC: Colour change; CS: Colour staining

The data presented in the table make it clear that when wool fabric was dyed using kachnar dye with addition of 0.25 per cent concentration of zinc oxide nanoparticles, the dye absorption was 21.32 per cent with 16.32 colour strength and fairly good (3/4) wash fastness grade for change in colour and good (4) wash fastness grade for colour staining. As the concentration of zinc oxide nanoparticles was increased from 0.50 to 1.00 per cent, the dye absorption raised from 23.96 to 27.78 per cent and colour strength from 17.58 to 19.44 displaying good (4) to excellent (5) wash fastness grades towards change in colour and colour staining respectively. While further increase in concentration of zinc oxide nanoparticles to 1.25 per cent, the dye absorption (27.13%) and colour strength (18.45) were noticed to be slightly decreased with very good (4/5) wash fastness rating for change in colour as well as colour staining.

Hence, on the basis of maximum per cent dye absorption and colour properties, one per cent concentration of zinc oxide nanoparticle was selected as optimum concentration for treatment of wool fabric and dyeing with kachnar dye. Khandual et al. (2015) reported that as the concentration of metal ions increases, they form a bridge between the functional groups of the dye and the wool protein and lead to higher dye exhaustion. Bhandari (2021) also selected 1.0 percent concentration of zinc oxide nanoparticle as optimum nanoparticle concentration on the basis of maximum percent dye absorption, highest colour strength (K/S) and wash fastness (CC) grades for dyeing of wool fabric with eucalyptus bark and madder root dyes.

iii. Optimization of nanoparticle treatment pH: The results related to optimization of pH for nanoparticle treatment are arranged in Table 6.

Table 6: Optimization of nanoparticle treatment pH on the basis of dye absorption and colour properties of dyed wool fabric

| Treatment pH | Nanoparticle treated dyed samples |  |  |  |
| --- | --- | --- | --- | --- |
|  | Per cent dye absorption | Colour strength (K/S) | Wash fastness grades |  |
|  |  |  | (CC) | (CS) |
| 4.5 | 32.09 | 22.34 | 4 | 4 |
| 5.0 | 32.58 | 21.76 | 4/5 | 4/5 |
| 5.5 | 33.23 | 23.48 | 5 | 5 |
| 6.0 | 31.67 | 22.32 | 4/5 | 4/5 |
| 6.5 | 29.24 | 20.57 | 4/5 | 4/5 |

CC: Colour change; CS: Colour staining

The data in the table clearly explain that when pH of zinc oxide nanoparticle treatment solution for dyeing of wool fabric with kachnar dye was maintained at 4.5, dye absorption was 32.09 per cent with 23.34 colour strength value and good (4) wash fastness grades towards change in colour and colour staining. As the pH of zinc oxide nanoparticle treatment solution was raised from 5.0 to 5.5 for simultaneous dyeing of wool fabric with kachnar dye, the dye absorption, colour strength and wash fastness grades were noticed to be increased from 32.58 to 33.23 per cent, 21.76 to 23.48 and 4/5 to 5 respectively. With progressive increase in the pH of zinc oxide nanoparticle treatment solution from 6.0 to 6.5, the per cent dye absorption and colour strength values were observed to be decreased from 31.67 to 29.24 per cent and from 22.32 to 20.57 respectively, exhibiting very good (4/5) wash fastness grades for colour change and colour staining.

Thus, 5.5 was selected as optimum treatment pH for zinc oxide nanotreatment and simultaneous dyeing of wool fabric with kachnar dye. Kiakhani et al. (2021) found that at acidic pH (4.0) the K/S values of sodium alginate-silver nanoparticle treated wool sample dyed with cochineal dye were higher than at neutral pH which indicated that the absorption process was mainly driven by electrostatic interaction between cochineal and positively charged wool fibres in acidic pH 4. Pratibha (2024) used 5.0 pH for treatment of silk fabric with the selected nanoparticles and dyeing with madder dye as the absorption of natural dyes on natural fibres depends on pH of dyeing bath therefore in acidic pH natural fibres form cationic groups, hence the exhaustion of natural dyes is higher in acidic medium.

iv. Optimization of nanoparticle treatment temperature: The data pertaining to optimization of nanoparticle treatment temperature are demonstrated in Table 7.

Table 7: Optimization of nanoparticle treatment temperature on the basis of dye absorption and colour properties of dyed wool fabric

| Treatment temperatures (°C) | Nanoparticle treated dyed samples |  |  |  |
| --- | --- | --- | --- | --- |
|  | Per cent dye absorption | Colour strength (K/S) | Wash fastness grades |  |
|  |  |  | (CC) | (CS) |
| 50 | 28.82 | 21.54 | 4/5 | 4/5 |
| 60 | 30.77 | 22.87 | 4/5 | 4/5 |
| 70 | 32.65 | 23.43 | 5 | 5 |
| 80 | 33.24 | 24.31 | 5 | 5 |
| 90 | 33.02 | 23.17 | 4/5 | 4/5 |

CC: Colour change; CS: Colour staining

It is clearly evident from the table that when zinc oxide nanoparticle treatment and simultaneous dyeing of wool fabric was carried out at 50℃ temperature, dye absorption was 28.82 per cent with 21.54 colour strength value and very good (4/5) wash fastness rating towards change in colour and colour staining. With increase in temperature from 60-80°C, the maximum dye absorption (33.24%) with highest 24.31 colour strength and excellent (5) wash fastness rating for change in colour and colour staining was acquired at 80℃ treatment temperature. The further increment in temperature to 90℃ slightly decreased the dye absorption to 33.02 per cent, colour strength to 23.17 and wash fastness (colour change and colour staining) to very good (4/5).

Hence, 80℃ temperature was found to be optimum temperature for imparting nanoparticle treatment and dyeing of wool fabric with kachnar dye. Xia and Tian (2010) highlighted that wool fibres are usually dyed under high temperature for long duration because of the dense scale structure and hydrophobic lipid layer covering the surface of wool fibres. Bhandari (2021) found 80oC to be optimum temperature for imparting nanoparticle treatment and simultaneous dyeing of wool fabric with eucalyptus bark and madder root dyes. Kiakhani et al. (2021) stated that the increment in colour strength of nano silver pretreated wool yarns was noticed when dyeing temperature was increased, probably due to achieving a faster dyeing equilibrium at elevated temperatures.

v. Optimization of nanoparticle treatment time: The per cent dye absorption, colour strength values and wash fastness grades obtained at different time durations are given in Table 8.

Table 8: Optimization of nanoparticle treatment time on the basis of dye absorption and colour properties of dyed wool fabric

| Treatment time (minutes) | Nanoparticle treated dyed samples |  |  |  |
| --- | --- | --- | --- | --- |
|  | Per cent dye absorption | Colour strength (K/S) | Wash fastness grades |  |
|  |  |  | (CC) | (CS) |
| 30 | 29.12 | 21.97 | 4 | 4/5 |
| 35 | 30.53 | 22.36 | 4/5 | 4/5 |
| 40 | 33.42 | 23.89 | 5 | 5 |
| 45 | 33.18 | 22.72 | 4/5 | 4/5 |
| 50 | 32.85 | 22.47 | 4/5 | 5 |

CC: Colour change; CS: Colour staining

It is observed from the table that when treatment of wool fabric with nano zinc oxide and simultaneous dyeing with kachnar dye was carried out for 30 minutes’ duration, 29.12 per cent dye absorption with 21.97 colour strength and good (4) wash fastness grade for colour change and very good (4/5) wash fastness grade for colour staining were observed. When nanoparticle treatment time was increased from 35 to 40 minutes, dye absorption of treated dyed samples increased from 30.53 to 33.42 per cent, colour strength values from 23.36 to 23.89 having very good (4/5) to excellent (5) wash fastness ratings for colour change and colour staining. The further progression in treatment duration from 45 to 50 minutes led to reduction in dye absorption (33.18 to 32.85%), colour strength values (22.72 to 22.47) with very good (4/5) wash fastness grade for colour change and very good to excellent (5) wash fastness grades for colour staining.

Hence, on the basis of maximum per cent dye absorption, highest colour strength and excellent wash fastness grades, 40 minutes duration was selected as optimum time for treatment of wool fabric with zinc oxide nanoparticle and simultaneous dyeing with kachnar dye. Muthu (2015) explained that mordanting of natural fibres for longer duration of time at moderate temperature can give good to excellent fastness properties. Khatib et al. (2022) reported that dyeing time is essential in characterizing the adsorbate and absorbent interactions. The dyeing time influenced the K/S values of TiO2 treated silk fabric dyed with alkanet dye, the increase in colour strength confirmed the positive effect of treatment time. Cheng et al. (2020) observed that absorption of Ag NPs and colour depth of silk fabric increased with increasing the treatment time and reached the highest level at 40 minutes.

vi. Optimization of material to liquor ratio of treatment bath: The data pertaining to different M:L ratio used for nanoparticle treatment and dyeing with kachnar dye are presented in Table 9.

Table 9: Optimization of M:L Ratio of treatment bath on the basis of dye absorption and colour properties of dyed wool fabric

| M:L Ratio | Nanoparticle treated dyed samples |  |  |  |
| --- | --- | --- | --- | --- |
|  | Per cent dye absorption | Colour strength (K/S) | Wash fastness grades |  |
|  |  |  | (CC) | (CS) |
| 1:20 | 32.19 | 21.82 | 4 | 4 |
| 1:30 | 33.42 | 22.65 | 5 | 5 |
| 1:40 | 33.65 | 24.12 | 5 | 5 |
| 1:50 | 32.29 | 23.86 | 4/5 | 4/5 |
| 1:60 | 31.53 | 22.61 | 4/5 | 4/5 |

CC: Colour change; CS: Colour staining

The table shows that when wool fabric was treated with zinc oxide nanoparticle and simultaneously dyed with kachnar dye keeping material to liquor ratio of 1:20, dye absorption was 32.19 per cent, colour strength value 21.82 and good (4) wash fastness grades for colour change and colour staining. With a rise in material to liquor ratio from 1:30 to 1:40, zinc oxide nanoparticle treated and kachnar dyed wool fabric samples exhibited the enhancement in dye absorption from 33.42 to 33.65 per cent, colour strength from 22.65 to 24.12 and wash fastness rating was same i.e. excellent (5) for colour change and colour staining. When M:L ratio was further raised from 1:50 to 1:60, reduction in dye absorption (32.29 to 31.53%), colour strength (23.86 to 22.61) value and very good (4/5) wash fastness ratings were noticed for nano zinc oxide treated and kachnar dyed silk fabric.

Therefore, 1:40 was selected as optimum M:L ratio for treatment of wool fabric with zinc oxide nanoparticle and simultaneously dyeing with kachnar dye. The results are in line with the findings of Sharma (2019) that maximum percent dye absorption for enzyme treated wool fabric was achieved at 1:40 M:L ratio. Pratibha (2024) used 1:50 M:L ratio for imparting nano aluminium oxide and nano titanium dioxide treatment to silk fabric and simultaneous dyeing with madder dye.

CONCLUSION

The present study demonstrates that kachnar dye, when combined with inorganic nanoparticles, offers a promising eco-friendly approach to wool dyeing. Although natural dyes traditionally face limitations such as low affinity and poor fastness properties, the incorporation of nanoparticles significantly enhances their performance. The nanoparticles act as effective mordants by increasing the surface interaction between dye molecules and wool fibers, resulting in improved dye uptake, higher color strength and better shade uniformity. Therefore, nano treatments can be imparted successfully to wool fabric with nanosized zinc oxide while dyeing with kachnar bark dye to improve the dyeability and colour fastness properties of the fabric. By incorporation of nanoparticles in dyeing, a range of brown to pinkish brown can be obtained with kachnar bark dye on wool fabric.

Disclaimer (Artificial intelligence)

Author(s) hereby declare that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc.) and text-to-image generators have been used during the writing or editing of this manuscript.

REFERENCES

- Muthu, S. S. (Ed.). (2015). Handbook of sustainable apparel production. CRC press.

- Ashique, S., Anand, K., Kumar, P., Dua, K., Chellappan, D. K. and Fatima, N. (2025). Dyes from natural products: characterization, chemical and biochemical analysis, and their importance. In Advances in Natural Dyes for Environmental Protection. Apple Academic Press, U.S.A. pp: 27-60.

- Barani, H., Boroumand, M. N. and Rafiei, S. (2017). Application of silver nanoparticles as an antibacterial mordant in wool natural dyeing: Synthesis, antibacterial activity and color characteristics. Fibers and Polymers. 18(4):658-665.

- Bhandari, V. (2021). Effect of metallic nanoparticles on dyeability of cotton and wool with natural dyes. Doctoral Thesis, CCS Haryana Agricultural University, Hisar.

- Cheng, T.H., Yang, Z.Y., Tang, R.C. and Zhai, A.D. (2020). Functionalization of silk by silver nanoparticles synthesized using the aqueous extract from tea stem waste. Journal of Materials Research and Technology. 9(3):4538-4549.

- Du, H., Yue, M., Huang, X., Duan, G., Yang, Z., Huang, W., ... & Yin, X. (2022). Preparation, application and enhancement dyeing properties of ZnO nanoparticles in silk fabrics dyed with natural dyes. Nanomaterials. 12(22):3953.

- Haijuan, D., Yue, M., Huang, X., Duan, G., Yang, Z., Huang, W., Shen, W. and Yin, X. (2022). Preparation, application and enhancement dyeing properties of ZnO nanoparticles in silk fabrics dyed with natural dyes. Nanomaterials. 12(22):1-11.

- Islam, S., Belowar, S., Das, S., Rahamatolla, M. and Datta, S. C. (2025). Chemistry of natural and synthetic dye materials with metal mordants in various fabrics for sustainable textile applications: a comprehensive review. Environmental Science and Pollution Research. 1-30.

- Khandual, A., Luximon, A., Sachdeva, C., Rout, N. and Sahu, P.K. (2015). Enhancement of functional properties of cotton by conventional dyeing with TiO2 nanoparticles. Material Today. 4(2):3674-3683.

- Khatib, E., Ngia, A., Nassar, S. and Nagla, E. (2022). Functionalization of natural fibres properties by using TiO2 nanoparticles to improve its antimicrobial activity. Biointerface Research in Applied Chemistry. 12(3):4177-4191.

- Kiakhani, M., Hashemi, E. and Gharanjig, K. (2019). Inorganic nanoparticles and natural dyes for production of antimicrobial and antioxidant wool fiber. Biotech. 9(12):456-460.

- Kiakhani, S.M., Safapour, S., Habibzadeh, S.A. and Bagha, T.A.R. (2021). Grafting of wool with alginate biopolymer/nano Ag as a clean antimicrobial and antioxidant agent: Characterization and natural dyeing studies. Journal of Polymers and the Environment. 29(3):2639-2649.

- Maulik, R.S., Chakraborty, L. and Pandit, P. (2021). Evaluation of cellulosic and protein fibers for coloring and functional finishing properties using simultaneous method with eucalyptus bark extract as a natural dye. Fibers and Polymers. 22(3):711-719.

- Mirnezhad, S., Sadeghi-Kiakhani, M. and Hashemi, E. (2023). Wool dyeing using Ziziphus bark extract as a natural dye: studies on the dyeing, antibacterial, and antioxidant characteristics. Environmental Science and Pollution Research. 30(18):51504-51517.

- Montazer, M. and Seifollahzadeh, S. (2011). Enhanced self‐cleaning, antibacterial and UV protection properties of nano TiO2 treated textile through enzymatic pretreatment. Photochemistry and Photobiology. 87(4):877-883.

- Pandey, R., Patel, S., Pandit, P., Nachimuthu, S. and Jose, S. (2018). Colouration of textiles using roasted peanut skin-An agro processing residue. Journal of Cleaner Production. 172(6):1319-1326.

- Pratibha. (2024). Natural dyeing of silk fabric using inorganic nanoparticles. Master’s Thesis, CCS Haryana Agricultural University, Hisar

- Rahman, M.S., Alom, J., Nitai, A., Hasan, M., Nam, S. and Mondal, M. (2022). Ultraviolet-blocking protective textiles. Protective Textiles from Natural Resources. Woodhead Publishing, Sawston, UK, (1):395-444.

- Rani, G., Bala, A., Ahlawat, R., Nunach, A. and Chahar, S. (2025). Recent advances in synthesis of AgNPs and their role in degradation of Organic dyes. Comments on Inorganic Chemistry. 45(1): 1-29.

- Rastogi, S. and Aggarwal, S. (2017). Dyeing of wool and silk fabrics with left over tea extract and tesu flower dye extract. International Journal for Environmental Rehabilitation and Conservation. 8(1):72-77.

- Rather, L. J., Shabbir, M., Ganie, S. A., Zhou, Q., Singh, K. P. and Li, Q. (2024). Natural dyes: Green and sustainable alternative for textile colouration. In Sustainable Textile Chemical Processing. CRC Press, pp. 41-69.

- Repon, M. R., Islam, T., Paul, T. K., Jurkonienė, S., Haji, A., Shukhratov, S. and Toki, G. F. I. (2024). Natural dyes in textile printing: parameters, methods, and performance. Environmental Science and Pollution Research. 31(35):47552-47583.

- Rukhaya, S. 2020. Microencapsulation of vetiver oil for development of aroma wool fabric. Master’s Thesis, CCS Haryana Agricultural University, Hisar.

- Sharma R. 2019. Effect of enzymatic treatment on dyeing of woolen fabric with natural dyes. Master’s Thesis, CCS Haryana Agricultural University, Hisar.

- Shokrzadeh, S., Razbin, M., Ghaheh, F. S., Tehrani, M. and Sadrjahani, M. (2025). Optimizing the eco-friendly dyeing of wool and nylon fabrics with Prangos ferulacea (L.) Lindl using artificial intelligence. Scientific Reports 15(1):13267.

- Singh, A. and Jahan, S. (2019). Extraction of natural dyes from Glycyrrhiza glabra and Lagerstroemia speciosa for wool dyeing and testing of its functional properties. International Journal of Current Microbiology and Applied Sciences. 8(12):2119-2129.

- Tangkawanit, S. and Keawsri, P. (2023). Silk fabrics coated ZnO nanoparticles and dyeing with natural indigo to enhance functional textiles. Suranaree Journal of Science and Technology. 30(1): 1-11

- Xia, F. and Tian, J. (2010). Study on dyeing properties of wool fabric under low temperature. In International Conference on Information Technology and Scientific Management, China, December, 20-21, 2010. pp: 263-266.

- Jiang, H., Guo, R., Mia, R., Zhang, H., Lü, S., Yang, F., ... & Liu, H. (2022). Eco-friendly dyeing and finishing of organic cotton fabric using natural dye (gardenia yellow) reduced-stabilized nanosilver: full factorial design. Cellulose, 29(4), 2663-2679.

- Memon, H., Khatri, A., Ali, N., & Memon, S. (2016). Dyeing recipe optimization for eco-friendly dyeing and mechanical property analysis of eco-friendly dyed cotton fabric: Better fixation, strength, and color yield by biodegradable salts. Journal of Natural Fibers, 13(6), 749-758.