# Application of Okra Seed Extract as Natural Coagulant for Clay Suspension Treatment in Alluvial Mining Wastewater

## ABSTRACT

Smaller-scale alluvial mining is a big source of water pollution in developing nations specifically Ghana, whereby the suspension clay minerals contribute in adding a lot of turbidity to water bodies. This work examines how the okra (Abelmoschus esculentus) seed extract is useful in the settlement of clay-filled mining wastewater by use of the raw extract as a natural coagulant. Three samples of clay (A, B and C) were made to 45 percent pulp density performance, and then natural settling and okra aided coagulation were performed under conditions pH-adjusted. The findings indicate that okra seed extract enhanced the settling rates by approximately three times in that the settling rates rose to 0.056 -0.102 m/s compared to initial rates of 0.019-0.036 m / s. The turbidity was reduced significantly, and it was found that it was reduced to 8.67-16.07NTU compared to 78.83221.17NTU. Altogether, the results prove the fact that okra seed extract is a promising treatment method of alluvial mining wastewater, a powerful, ecologically friendly, and inexpensive alternative to commercial chemical coagulants, and it can have a significant impact in terms of its use in resource-restrained settings.

Keywords: Natural coagulant, okra seed, clay suspension, alluvial mining, water treatment, turbidity reduction

## 1. INTRODUCTION

### 1.1 Background

Availability of clean drinking water is a very serious problem in the developing countries especially in places that are impacted by the activities of the small-scale mining (Aryee et al., 2003). Alluvial mining activities that take place at the banks of rivers in Ghana and other West African nations have played a major role in the degradation of water quality by the release of the clay-loaded tailings into the water bodies. They are suspended clay particles, generally less than 0.004 mm diameter making colloidal suspensions which are hard to settle by natural means because of the electrostatic charge and the low specific gravity (Adetuyi & Osagie, 2011) which renders the usual process of settling to be inefficient unless under the action of a chemical.

Alluvial mining, whereby minerals are mined in the sedimentary deposits in the rivers and streams has grown at an alarming rate over the past few decades. Although this activity offers economy to the local communities, it has left a devastating impact on the environment (especially water contamination). Ghana has also witnessed significant degradation of rivers like the Pra, Densu and Ankobra which not only impacted on aquatic biodiversity in the rivers but also had implication on human beings who used the rivers as their sources of water. The issues presented demonstrate that it is necessary to find safe, inexpensive and ecologically-friendly methods of treatment that can be adopted in communities affected by mining.

### 1.2 Problem Statement

The traditional method of treatment of turbid water is the use of chemical coagulants like polyaluminum chloride and aluminum sulfate (alum). There are, however, a number of disadvantages associated with the synthetic coagulants: they are costly to those communities that are resource constrained and they produce a sludge that is dangerous due to the presence of the residual aluminum, and may lower water pH, especially in low temperatures. Further, the long-term environmental costs of the aluminum-based coagulants have cast doubt on their applicability in water management of the 21st century in a sustainable manner.

Dialysis encephalopathy and other health conditions are one of the problems that concern people about the possible correlations to the accumulation of aluminum in the treated water. Moreover, there is a problem of disposing aluminum rich sludge, which pose environmental problems, as the substances may accumulate in the ecosystem, and they may find their way into food chains. Such restrictions demand the search of other more sustainable coagulation technologies.

### 1.3 Rationale for Natural Coagulants

Plant coagulants have shown good potentials as alternatives to chemical coagulants. In order to lower toxic sludge generation, minimal toxic content, most of these bio-based materials are biodegradable, locally sourced and inexpensive, and do not have negatively affecting environmental impacts. Okra (Abelmoschus esculentus) is among other natural coagulants being studied in the world because it is a polysaccharides and a polymers of similar nature formed by sticky gel which is a polysaccharide and also natural polymers facilitating the binding of particles.

### 1.4 Research Objectives

This paper has attempted to determine the success rate of okra seed extract as a natural coagulant to settle suspended clay vested in alluvial mining waste water. Certain goals encompassed: numerically testing improvements in settling rate resulting with okra seed treatment, efficiency to reduce turbidity, a determination of optimal pH conditions to coagulant, and individual compositions of clay samples.

## 2. MATERIALS AND METHODS

### 2.1 Sample Collection and Preparation

Three clay samples were obtained at various small-scale alluvial mines in Ghana referring to the following sample names; Sample A (AKY site), Sample B (KOLAK site), and Sample C (BSDT site). The areas were chosen to symbolize the common mines that have an impact on the available sources of water.

Each site had a representative 20 kg bulk sample collected according to the conventional sampling procedures. The samples were sieved to obtain 80% passing 38 µm sieve size, which was consistent across all the experimental trials in terms of the distribution of the particle size. Experimental procedures were made on 1 kg representative portions of each bulk sample by means of standard quartering.

### 2.2 Coagulant Preparation

Seeds of fresh okra were obtained in Tarkwa local markets in Ghana. The preparation procedure consisted of: full washing to eliminate impurities and debris, sun drying over 24 hours at ambient temperatures of between 28-32oC, mortar and pestle grinding to obtain fine powder and sieving to eliminate bigger particles to achieve homogeneity.

The powder which resulted was kept in sealed containers at room temperature. Each run of the experiment used 1g of the stock sample of okra seed powder.

### 2.3 Experimental Design

#### 2.3.1 Pulp Preparation

All settling tests were conducted at 45% solid concentration, calculated as follows:

For total volume of 250 mL:

- Mass of solid = ρ × (250 - X) mL

- Where X = volume of water

- Percent solid = 45%

This concentration was selected to simulate typical tailings densities encountered in small-scale mining operations while ensuring reproducible results.

#### 2.3.2 Natural Settling Tests

#### Early settlement condition was defined in natural conditions:

- 80 g of the samples each were added to 220 mL of fresh water.

- Mixes were pipetted (2 times) into graduated cylinders (250 mL).

- Natural pH was taken with the help of a calibrated pH meter.

- Settling interface height was measured at time intervals that included 0, 2, 4, 6 and 8, 10, 15, 20, 25, 30, 40, 50, 70 and 90 minutes.

#### Initial turbidity was measured with the help of turbidity meter.

#### 2.3.3 Coagulation Tests

### To assist the settling by coagulant:

- Fresh samples were made at a solid concentration of 45% fresh.

- The pH was then brought to a value of around 10.7 by adding 0.85 g lime (CaO).

- Ascent: 1 g okra seed powder was put in each sample.

- Mixtures were stirred by hand during 30 seconds in order to have homogeneous distribution.

- Settling interface was observed in identical intervals.

- Final turbidity was determined after 90 minutes.

### 2.4 Analytical Methods

## pH Measurement: In this case, the measurement was performed with the help of a calibrated digital pH meter (precision within spotted potassium deficiencies = -++) right after pulp preparation or after the lime was treated.

## Turbidity Analysis: Turbidity and clarity were determined by use of nephelometric turbidity meter using the formazin standards in Nephelometric Turbidity Unit (NTU).

## Calculation of Settling rate: It was calculated by observing the slope of the height versus time plots in the first linear settling period, which is in meters per second (m/s).

## The possible disadvantage of this arrangement is that large scale industrial flows might not be completely recreated in the laboratory settling conditions and additional pilot scale studies are suggested.

## 3. RESULTS

### 3.1 Initial Sample Characterization

#### 3.1.1 Natural pH

The pH of the natural samples of clay was found to be between 6.7 and 6.9 that is to say slightly acidic and near-neutral conditions:

Table 1: Showing the Natural pH of the Various Samples

| Sample | Natural pH |
| --- | --- |
| A | 6.8 |
| B | 6.7 |
| C | 6.9 |

The pH values are typical of a clay mineral which contains silica and other metal oxides and the chemical composition of the sedimentary minerals are reflected in the natural chemical composition.

The knowledge of natural pH can also be used to know the degree of conditioning that should be achieved in order to maximize the performance of the natural coagulants.

#### 3.1.2 Initial Turbidity

Significant variation in initial turbidity was observed across samples:

Table 2: Turbidity before Coagulation.

| Sample | Initial Turbidity (NTU) |
| --- | --- |
| A | 78.83 |
| B | 99.17 |
| C | 221.17 |

### Sample C had almost triple the turbidity of Sample A, which indicates that there are variations in the composition of clay mineral and particle size distribution or surface chemistry. Initial turbidity has a great effect on coagulant requirement as well as settling efficiency.

### 3.2 Natural Settling Behavior

Under natural conditions without coagulant, all samples demonstrated slow settling rates characteristic of fine clay suspensions:

Chart 1: Comparison of Settling Behavior of Suspended Particulate Samples

| Sample | Settling Rate (m/s) | Time for 50% Settling (min) |
| --- | --- | --- |
| A | 0.019 | >50 |
| B | 0.021 | >50 |
| C | 0.036 | ~40 |

The 20 minute initially steep, then much slower settling rates were observed in the patterns. Sample C showed the fastest natural growth rate, although it had the greatest turbidity, which could be attributed to a bigger aggregate particle size or a dissimilar composition of clay mineral. The accelerated natural setting of Sample C can be explained by a larger value of the particulate concentration, which enhances aggregation.

### 3.3 pH Conditioning Effect

Addition of 0.85 g lime increased pH to optimal alkaline conditions:

Table 3: Showing the pH After Conditioning

| Sample | pH After Conditioning |
| --- | --- |
| A | 10.77 |
| B | 10.70 |
| C | 10.65 |

### The raised pH is essential in okra seed coagulants because higher pH favorable ionization of active polymeric substances as well as neutralizing clay particle charges.

### 3.4 Coagulation Performance

#### 3.4.1 Settling Rate Enhancement

Addition of okra seed coagulant dramatically improved settling rates:

Table 4: Setting rate before and after coagulation

| Sample | Before Coagulation (m/s) | After Coagulation (m/s) | Enhancement Factor |
| --- | --- | --- | --- |
| A | 0.019 | 0.059 | 3.1× |
| B | 0.021 | 0.056 | 2.7× |
| C | 0.036 | 0.102 | 2.8× |

The greatest impact was experienced in the initial 15 minutes following the agitation of coagulant, at which point the rate of settling was found to increase significantly. A period later, the settling rate became stable, which means that the primary process of the coagulation-flocculation process was finished.

Figure 1: Showing the Settling Rates Before and After Coagulation

#### 3.4.2 Turbidity Reduction

Turbidity decreased dramatically following okra seed treatment:

Table 5: Turbidity before and after coagulation

| Sample | Before (NTU) | After (NTU) | Reduction (%) |
| --- | --- | --- | --- |
| A | 78.83 | 11.57 | 85.3% |
| B | 99.17 | 16.07 | 83.8% |
| C | 221.17 | 8.67 | 96.1% |

Sample C that had the highest turbidity initially recorded the highest absolute and relative turbidity reduction. This implies that okra seed coagulant is specifically used on highly turbid waters, where the concentration of the suspended particles enhances bridging of the particles.

## 4. DISCUSSION

### 4.1 Mechanisms of Coagulation

### The mechanism of coagulation of okra seed extract may be explained by a number of processes:

### Charge Neutralization: Cationic proteins and polysaccharides which occur in okra seeds neutralize the negative surface charges on clay particles. Clay minerals are normally negative charged because of an isomorphic replacement of the mineral structure, and ionization of the hydroxyl groups that are attached to the surface.

### Polymer Bridging: The polymers in the mucilaginous coats of okra seeds are long-chain polymers that simultaneously bind to various clay particle creating bridges to form bigger and more quickly settling flocs.

### pH-Dependent Activity: Alkalinity produced by the lime addition increases the solubility and activity of the active compounds of okra to enhance their reaction towards clay surfaces.

### 4.2 Comparison with Conventional Coagulants

Although, no direct comparisons to aluminum-based coagulants were done in this study, literature indicates that natural coagulants such as okra can perform similarly under favorable circumstances. This increase in settling rate of 3 times and over 80 percent removal of turbidity improvement is also in line with or even greater performance of some traditional coagulants at the same dosage.

### Other comparable achievements have been reported with the use of moringa oleifera and cactus mucilage in water treatment systems of community scales.

### The major benefits of okra seed coagulant are:

- Safety: No residues of toxic metals in treated water and sludge.

- Biodegradability: Organic sludge is able to occur naturally.

- Local availability: The okra is widely grown in the tropical areas.

- Cost effectiveness: Completely inexpensive compared to foreign chemical coagulants.

- Features: Does not need a lot of processing machinery.

### But the okra extract unlike coagulants made out of aluminum does not leave behind traces of metals such as aluminum and hence it is less unsafe over the long-term application in the environment.

### 4.3 Sample Variability and Implications

The varying reactions of the three clay samples stress on the relevancy of mineralogical composition in the coagulation efficiency. The better response of Sample C can be because of:

- Diversity: types of clay mineral (e.g. more smectite)

- Disagreements in particle size distribution.

- The dissimilarity of organic matter concentrations.

- Various binding capacities of cation exchanges.

This inconsistency implies that the best dosage levels of the coagulant can be determined by site-specific calibration, but the overall performance in all samples is promising in feasibility to be used in the field.

### 4.4 Practical Applications

### The implications of the findings are important to the small-scale mining operations:

### Water Recycling: Treated water would have a chance to be recycled to be used in mining operations, and it would decrease the amount of fresh water and environmental emissions.

### Community Water Treatment: Community level water treatment might also be introduced using simple okra-based treatment systems to treat the affected water sources.

### Regulatory Compliance: Natural coagulation would potentially assist the mining industry to comply with the environmental standards akin to water discharge.

### Scalability: This approach is simple to prepare and apply and therefore it can be used in operations of any scale.

### 4.5 Limitations and Challenges

### There are a number of issues that have to be hurdled to adopt them on a large scale:

### Seasonal Availability: Okra supply could be seasonal and therefore needs storage policies.

### Dosage Optimization: It requires further research, which can determine optimum dosing protocols to operate with different qualities of water.

### Microbial Growth: Organic coagulants can promote bacteria growth; timely or corresponding care should be subjected to treated water.

### Mechanism Understanding: Greater efforts to get molecular interactions optimized would be aided by more careful research.

### 4.6 Economic and Environmental Considerations

Okra seed coagulant is economically viable and this quality is compelling to resource-constrained environments. Local farming of okra offers a source of employment and farm production and solves the environmental issues. The biodegradation of the treatment residue also removes expensive sludge disposal facilities that are involved in the aluminum-based systems.

As far as environmental benefits are concerned, they are not limited to waste reduction. Okra coagulation can minimize the impact of the mining industry on the natural water bodies by catalyzing the effective on-site treatment of the water that can help in the restoration of the ecosystems.

## 5. CONCLUSIONS

In this study, the authors were able to prove that okra seed extract can be used as a natural coagulant to blindly treat clay-contaminated wastewater in alluvial mining processes. Key findings include:

- In all samples that were tested, okra seed powder enhanced the rate of clay settling 2.7-3.1 times.

- In all cases, turbidity reductions of over 83 percent were obtained and in others, reductions of up to 96 percent were obtained.

- conditioning to high PH (pH =10.7) improved the coagulant performance.

- The coagulant was more effective within the initial 15 minutes of treatment.

- Best relative improvement was achieved with sample of high initial turbidity.

These findings prove okra seed extract as an alternative coagulant that is viable and sustainable, and can be widely used in developing areas where mining is observed to compromise the quality of water. This renders okra seed extract an effective target to the decentralized or community-based water treatment systems in mines-affected areas. The treatment is both environmentally, economically, and health-beneficial when compared to the aluminum-based treatments, and is also employing the locally available renewable resources. To ensure its performance in other environment and operating conditions, future field tests are necessary to confirm the validity of its performance.

## 6. RECOMMENDATIONS

Future studies are required to coherently examine the dosage of okra seeds used in the dosage of 0.5-2.0 g per 250 mL of pulp on coagulator power and also the impact of pH within the alkaline pH range 8-12. Special attention should be paid to the best time of coagulant application, the stirring strength and period of dispersion and extraction of active components with 0.1 M NaCl solution or dry powder of the solution, as these parameters will likely influence the process of floc development and settling characteristics. SEM analysis of the flocs would help as an effective way to see a visual evidence of charge neutralization and polymer-bridging. Simultaneously, a close description of the flocculating polysaccharides and proteins in okra seeds, along with mineralogical modification of the clay samples (especially in smectite content and cations exchange capacity), would make it clearer that coagulation efficiency varied at sites. It should also be quantified whether the stored okra seed powder is stable or subject to seasonal changes to make certain it is reliable all year round.

To be practically applied in the field, standard operating practices, i.e., the use and preparation of okra seeds equip with clear and illustrated procedures should be crafted and spread. The small-scale miners training programmes must be increased and the processing centres set up at community levels in order to ensure quality coagulant supply at all times. Low cost, simple settling units to suit remote mining must be designed and proved out at pilot scale in an active alluvial mining project to prove they are practical in greater throughput. Setting quality standards on the preparation of okra seed powder will lead to more adoption and trust of the operators.

Governments at policy level ought to establish incentives and regulations that support sustainable practices in water-treatment such as the official acknowledgement of natural coagulants in environmental policies. Uptake will be enhanced by supporting the local research and extending service provision along with incorporating of indigenous plant-based technologies into national water policies and mining policies. Further encouragement of okra as a food crop and water-treatment resource in the mining-impacted areas, should be seen as an effective approach to ensuring that agricultural development and environmental protection missions in those areas do not conflict.

Disclaimer (Artificial intelligence)

Option 1:

Author(s) hereby declare that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc.) and text-to-image generators have been used during the writing or editing of this manuscript.

Option 2:

Author(s) hereby declare that generative AI technologies such as Large Language Models, etc. have been used during the writing or editing of manuscripts. This explanation will include the name, version, model, and source of the generative AI technology and as well as all input prompts provided to the generative AI technology

Details of the AI usage are given below:

1.

2.

3.

## REFERENCES

Adetuyi, F., & Osagie, A. (2011). Nutrient, antinutrient, mineral and zinc bioavailability of okra Abelmoschus esculentus (L) Moench Variety. American Journal of Food and Nutrition, 1(2), 49–54. https://doi.org/10.5251/ajfn.2011.1.2.49.54

Aryee, B. N. A., Ntibery, B. K., & Atorkui, E. (2003). Trends in the small-scale mining of precious minerals in Ghana: A perspective on its environmental impact. Journal of Cleaner Production, 11(2), 131–140. https://doi.org/10.1016/S0959-6526(02)00043-4

Carneiro-Marra, L., Sad, L., & Da Silva-Batista, M. (2019). Evaluation of mucilage and powder of Okra as bio-flocculant in water treatment. Revista ION, 32(2), 53–58. https://doi.org/10.18273/revion.v32n2-2019005

De Jesus, E., Victor Cruz, P., Adair Pacífico, J., & Santos Silva, A. (2014). Removal of Turbidity, Suspended Solids and Ions of Fe from Aqueous Solution using Okra Powder by Coagulation-Flocculation Process. American Journal of Water Resources, 1(3), 20–24. https://doi.org/10.12691/ajwr-1-3-1

Deng, X., Yang, H., Liu, Y., Cheng, J., Yang, C., & Liu, J. (2025). Exploring the dynamics of Southern Hemisphere westerlies using abrupt warming and cooling experiments. In Review. https://doi.org/10.21203/rs.3.rs-7873277/v1

Kaur, A., Sangha, M. K., Devi, V., Pathak, M., & Kaur, N. (2025). Nutritional and mineral profiling of wild okra (Abelmoschus esculentus) seeds accessions: Insights into seed composition. Heliyon, 11(13), e43759. https://doi.org/10.1016/j.heliyon.2025.e43759

Massrie, K. D. (2025). Constraints and opportunities on okra (Abelmoschus esculentus) production in Ethiopia: A review. Frontiers in Sustainable Food Systems, 9, 1546995. https://doi.org/10.3389/fsufs.2025.1546995

Maycock, A. L., Abeles, R. H., Salach, J. I., & Singer, T. P. (1976). The structure of the covalent adduct formed by the interaction of 3-dimethylamino-1-propyne and the flavine of mitochondrial amine oxidase. Biochemistry, 15(1), 114–125. https://doi.org/10.1021/bi00646a018

Muthuraman, G., & Sasikala, S. (2014). Removal of turbidity from drinking water using natural coagulants. Journal of Industrial and Engineering Chemistry, 20(4), 1727–1731. https://doi.org/10.1016/j.jiec.2013.08.023

Parra, A., Morales, N., Vallejos, J., & Nguyen, P. M. V. (2018). Open pit mine planning considering geomechanical fundamentals. International Journal of Mining, Reclamation and Environment, 32(4), 221–238. https://doi.org/10.1080/17480930.2017.1278579

Shristee Mishra, Singh, S., & Ruchira Srivastava. (2019). Okra Seeds: An Efficient Coagulant. Unpublished. https://doi.org/10.13140/RG.2.2.30299.92967

Szynkarczuk, J., Kan, J., Hassan, T. A. T., & Donini, J. C. (1994). Electrochemical Coagulation of Clay Suspensions. Clays and Clay Minerals, 42(6), 667–673. https://doi.org/10.1346/CCMN.1994.0420602