UNRAVELING THE PSEUDO GAP PHASE IN CUPRATE SUPERCONDUCTORS: EXPERIMENTAL SIGNATURE, THEORETICAL FRAMEWORKS, AND ITS ROLE IN HIGH TEMPERATURE SUPERCONDUCTIVITY

ABSTRACT:

Among the various mysteries in cuprate high temperature superconductors, the pseudogap (PG) phase stands out for the difficulty in pinning down its origin and its close connection to unconventional superconductivity. It appears above the superconducting transition temperature TC​, where part of the low energy spectral weight becomes depleted and several competing or intertwined orders such as charge and pair density waves, nematicity, and spin fluctuations begin to develop. A persistent challenge lies in the systematic discrepancies revealed by different experimental probes, as transport measurements locate the critical doping near p*≈0.18-0.19, spectroscopic studies around p*≈0.22, and symmetry sensitive techniques close to p*≈0.23. These variations reflect the distinct sensitivities of each probe to correlation length scales and electronic coherence rather than experimental inconsistency.

This review brings together evidence from angle resolved photoemission spectroscopy (ARPES), scanning tunneling microscopy or spectroscopy (STM or STS), nuclear magnetic resonance (NMR), resonant X ray scattering (RXS), and optical conductivity, showing that the pseudogap is a spatially heterogeneous, symmetry breaking electronic state whose onset temperature T* decreases roughly linearly with doping and terminates sharply at p*. Three complementary theoretical frameworks, namely quantum criticality, Mott physics, and intertwined orders, collectively describe these observations. Experiments showing the abrupt disappearance of nematic order and a logarithmic rise in the electronic specific heat coefficient Cel/ T suggest that the pseudogap terminates at a quantum critical point. This transition appears to separate a correlation dominated pseudogapped metal from a coherent Fermi liquid phase rather than occurring through a gradual crossover. The doping level identified from transport data aligns with optimal superconductivity, implying that the recovery of long range phase coherence rather than the complete removal of pseudogap features is what ultimately enhances TC.

Unresolved questions include reconciling probe dependent boundaries through systematic cross technique studies on identical crystals and developing correlation length resolved probes to distinguish spatial scales of electronic reconstruction. A major theoretical challenge remains to unify competing frameworks and to elucidate how the pseudogap terminates and coherence emerges at p*, which represents a key step toward a microscopic theory of high temperature superconductivity in cuprates.

Keywords: Pseudogap, High-temperature superconductivity, Cuprates, Charge density wave (CDW), Nematicity, Phase diagram, Scanning tunneling microscopy (STM), Quantum criticality.

## 1.0 INTRODUCTION

High-temperature superconductivity in cuprates remains one of the central challenges in condensed matter physics [1]. Despite decades of intensive study, its microscopic mechanism is still unresolved [2]. Recent experimental and theoretical progress has highlighted the pseudogap (PG) as a key player in this puzzle, linking it directly to the emergence of superconductivity (SC) [3]. The PG represents a mysterious phase [4], characterized by a partial depletion of low-energy electronic states between the superconducting transition temperature TC and a higher onset temperature T*[5, 6]. Unlike conventional ordered phases, it lacks a universally accepted order parameter and displays unconventional signatures across probes [7, 4].

Thermodynamic studies establish that the PG terminates sharply at a critical doping level p* [7], beyond which a strange metallic state emerges [8]. This boundary suggests the PG is not merely a crossover but a distinct quantum phase. The phase diagram in Figure 1 illustrates this landscape - the PG spans from the antiferromagnetic (AFM) insulator to p*, with the superconducting dome embedded inside [7,8]. This visual framework supports theoretical proposals that the PG reflects a broken-symmetry phase with its own identity [9, 10].

Figure 1: Schematic phase diagram of cuprate superconductors showing temperature versus hole doping concentration. Key phases include the antiferromagnetic (AFM) insulator, pseudogap region, superconducting dome, and metallic state. Critical points are marked: ps (onset doping), pc (optimal doping), and p*  (critical doping), with temperature scales TN  (Néel temperature), Tc (superconducting transition temperature), and T* (pseudogap onset temperature), Adapted from [11].

A major challenge lies in reconciling discrepancies between experimental probes, where transport studies suggest p*≈0.18-0.19 [12], spectroscopic measurements yield p*≈0.22 [13], while symmetry-breaking studies report p*≈0.23 [14]. These systematic differences likely reflect distinct spatial and dynamical sensitivities rather than experimental uncertainty. Temperature scaling is also material-dependent, yet often follows a universal relation: T*∝p*-plinking the doping and onset temperature [15, 16].

Theoretical frameworks propose that the PG reflects a quantum phase transition. Research points to a crossover from a doped Mott insulator with resonating-valence-bond (RVB) spinon pairing to a fragile BCS-like Fermi liquid, consistent with the observed breakdown of d-wave superconductivity near p* [9]. Competing interpretations attribute the PG to hidden magnetism [17], short-range spin correlations [5], and quantum critical fluctuations [10]. In contrast [6] argues for an intertwined origin involving spin, charge, and superconducting orders, suggesting the PG is not a single mechanism but a composite phase.

Notably, the collapse of the PG at p*coincides with enhanced spin fluctuations, a peak in specific heat, and the onset of strange metallicity [10]. Taken together, these results reinforce the view that the PG is a distinct quantum phase tied to criticality which is central to understanding the unconventional superconductivity of cuprates [9, 10].

## 2.0 EXPERIMENTAL SIGNATURES OF THE PSEUDOGAP

### 2.1. Angle-Resolved Photoemission Spectroscopy (ARPES)

ARPES provides direct, momentum-resolved insights into the PG, revealing how its anisotropic gap structure and quasiparticle coherence reflect the influence of strong many-body interactions in cuprates [18]. In electron-doped cuprates such as Pr1.3-xLa0.7CexCuO4, evidence in [18] shows that the PG opens across the unfolded Fermi surface while leaving nodal regions largely intact. The gap magnitude increases from the diagonal toward the antinode, a behavior which is inconsistent with simple AFM band-folding but in agreement with cluster dynamical mean-field theory (CDMFT), which attributes the gap to strong electronic correlations [18].

Complementary theory using the Two-Particle Self-Consistent (TPSC) approach to the two-dimensional Hubbard model shows that an increasing spin correlation length produces a momentum-dependent PG concentrated at antinodes [19]. The TPSC self-energy is

### σ(2)k,iωn=Un-σ+TNU8 q,iΩm[3Uspχsp(q,iΩm)+ Uch χch(q,iΩm)] G1(k+q,iωn+iΩm)

Where U is the Hubbard interaction strength, Usp(ch) are renormalized spin (charged) vertices, χsp(ch)q,iΩm represents the corresponding spin susceptibilities, G1is the first level Green’s function [20] and the spectral function follows:

### Ak,ω=-1π Im1ω+μ-ℇk-(k,ω+i0+)

### Where μ is the chemical potential, and ℇk is the band dispersion [21]. ARPES data show d-wave momentum dependence:

### ΔPGk=Δ0cos kx-cos ky2

Where  kx and ky are momentum components and Δ0 sets the gap scale [22]. This consistency between experiment and theory underscores the central role of short-range spin correlations in shaping PG behavior. Figure 2, provides direct experimental evidence for this theoretical framework, showing spectral intensity maps where the predicted antinodal suppression is clearly visible while nodal regions remain largely unaffected. The momentum selectivity demonstrated in these ARPES measurements confirm the correlation-driven mechanisms discussed above [18, 23].

Figure 2: Momentum-resolved ARPES spectra from Bi2201 at T = 10 K showing evolution from nodal (cut #1) to antinodal (cut #5) directions. (A) Fermi surface mapping with measurement cuts indicated. (B-F) Energy-momentum dispersion showing spectral weight suppression and band flattening near antinodes. (G-K) Evolution with doping demonstrating momentum-selective pseudogap behavior. Intensity scale from low (L) to high (H). Adapted from [18].

Additional ARPES studies report antinodal spectral-weight suppression, Fermi-momentum misalignment and asymmetric broadening that resist pure CDW/SDW explanations; combined strong-correlation plus Fröhlich EPI models reproduce these anomalies [23]. Importantly, ARPES observes PG closure at p*≈0.22 higher than transport values, reflecting its sensitivity to local electronic structure beyond long-range coherence scales [13].

### 2.2. Scanning Tunneling Microscopy/Spectroscopy (STM/STS)

STM/STS provides atomic-scale access to the electronic structure of cuprates, revealing spatial modulations, charge order, and symmetry breaking within the PG regime [24]. In Bi-based cuprates (Bi-2212, Bi-2201), STM detects checkerboard charge density wave (CDW) patterns emerging near the PG energy scale ∆*[24, 25]. In overdoped (Bi,Pb)2Sr2Cu06+x, these CDW signatures peak at ∆*, firmly linking them to the PG [24, 25].

Spatial variations of the local density of states (LDOS) are well described by

ρr,ω=ρ0ω+jAjωcos⁡(Qj.r+ϕjω)

Where ρ0ω represents the spatially averaged background density of states, Ajω denotes the energy-dependent modulation amplitude for wavevector Qj, and ϕjω captures phase shifts that reflects the underlying electronic correlations [26].Initially modeled as simple cosine modulations [26], this framework has since been generalized to capture local amplitude and phase anisotropies along distinct crystallographic axes [24].

Topological defects such as vortices with winding number ±1 have been observed in CDW patterns of overdoped Bi-2201, suggesting local strain, inhomogeneity, and fluctuating order [24]. Furthermore, a vestigial nematic state has been identified in Bi-based cuprates, characterized by intra-unit-cell rotational symmetry breaking that coexists with CDW correlations [27]. Together, these results show that the PG phase is spatially heterogeneous, symmetry-breaking, and intertwined with charge order and doping [24, 25, 27].

Importantly, STM detects PG and CDW features persisting well beyond transport-based critical doping. In Bi-2201, CDW correlations survive up to p*≈0.21 [24], exceeding transport estimates of p*≈0.18-0.19 [12]. This highlights STM’s unique sensitivity to nanoscale electronic reconstruction even after bulk coherence is restored.

Figure 3: STM/STS measurements showing spatial heterogeneity of pseudogap energy in Bi-based cuprates. (A) dI/dV spectra at different spatial positions on underdoped (UD60K), underdoped (UD70K), and optimally doped (OP91K) samples, with vertical offset for clarity. Gray lines indicate gap values Δ. (B) Effective charge measurements showing systematic evolution with bias voltage, with error bars representing standard deviation. Dashed lines indicate reference levels. (C) Correlation plot of pairing energy EPG vs gap magnitude  ∆PG across different doping levels, demonstrating the systematic relationship between local electronic properties and pseudogap behavior. Adapted from [4].

Figure 3 demonstrates the spatial heterogeneity of PG properties revealed by these STM/STS measurements. The systematic correlation between local pairing energies and gap magnitudes across different doping levels confirms the intricate relationship between charge order and PG physics established in the preceding analysis [24, 27].

### 2.3. Nuclear Magnetic Resonance (NMR)

NMR probes local magnetic environments and has yielded decisive insights into the PG phase through the Knight shift and spin-lattice relaxation rate 1T1​ [28]. In underdoped cuprates, both quantities drop sharply below T*, signaling reduced spin susceptibility and a gapped spin excitation spectrum [28, 29]. The PG is strongly doping-sensitive and largely temperature-independent; in theoretical extrapolations, its energy scale may extend up to ~1500 K in highly underdoped systems, although experimental estimates for specific cuprates remain in the few hundred Kelvin range [28]. Doping studies reveal that decreasing hole concentration enhances AFM correlations within CuO2  planes, reinforcing PG signatures in Knight shift and 1T1​ data [28]. A two-component model reconciling coexisting metallic and AFM domains captures this doping evolution [29].

Earlier homogeneous models have given way to real-space frameworks that capture atomic-scale inhomogeneity, resolving discrepancies in temperature dependence and aligning with STM observations of nanoscale order [29, 24, 27]. Overall, NMR demonstrates that the PG is doping-sensitive, spatially inhomogeneous, and robust against thermal fluctuations, hallmarks of a distinct broken-symmetry phase.

### 2.4. Resonant X-ray Scattering (RXS) and Resonant Inelastic X-ray Scattering (RIXS)

RXS and RIXS have provided decisive momentum-resolved insights into charge correlations and symmetry breaking in cuprates [30, 31]. In La1.6-xNd0.4SrxCuO4 (Nd-LSCO), RXS revealed that electronic nematicity is fundamentally linked to the PG regime, with nematic order vanishing at the critical doping p*=0.23±0.01 [14]. This marks the upper bound of PG-related phenomena, highlighting local symmetry breaking as the most persistent signature of electronic reconstruction, persisting beyond thresholds observed in transport and spectroscopy. Complementary RIXS studies uncovered short-range charge density fluctuations that survive up to room temperature, well above T* [30, 2]. These fluctuations are dynamic, doping- and temperature-dependent, and vanish only at the PG endpoint p*, underscoring their connection to quantum criticality [14, 2, 30-31]. Collectively, RXS and RIXS establish nematicity and charge density fluctuations as robust hallmarks of the PG phase.

### 2.5 Optical Conductivity and Spectroscopic Signatures

Optical conductivity measurements reveal fundamental aspects of the PG phase in underdoped cuprates, demonstrating anomalous spectral weight redistribution that distinguishes it from conventional superconductors [32, 33]. Unlike conventional systems where spectral weight is simply redistributed due to pairing, cuprates exhibit fundamental reorganization across energy scales, indicating deep-seated many-body correlations that extend far beyond the superconducting gap energy [32].

The spectral weight redistribution in cuprates is particularly striking, extending up to 1eV in the infrared region far exceeding what would be expected from simple cooper pairing mechanisms [33]. This anomalous behavior suggests that the PG involves complex electronic reorganization that may reflect underlying nanoscale inhomogeneity rather than uniform gap formation [32]. The PG phase exhibits characteristics of incipient pairing without long-range coherence, manifesting as a "two-fluid" state where coherent and incoherent components evolve independently [33].

Infrared spectroscopy provides direct evidence for this decoupling, revealing that quasiparticle coherence and pairing strength follow distinct temperature and doping dependencies within the PG regime [33]. The spectral weight conservation requires:

WΩc=0Ωcσ1ω dω

Where σ1ω is the real optical conductivity, WΩc is the integrated spectral weight and Ωc sets the infrared cutoff (Ωc≈1eV) [34, 33]. Remarkably, the electronic kinetic energy decreases in the superconducting state opposite to BCS theory predictions indicating a fundamental breakdown of conventional SC models in the underdoped regime [32].

2.5.1 Doping Evolution of Spectroscopic Signatures

Systematic optical spectroscopy reveals how PG features evolve with doping toward the critical concentration p* [33]. In LSCO and Eu-LSCO, the coherent Drude spectral weight K* increases steadily, reflecting enhanced carrier coherence as the system approaches a more metallic state [35, 33]. Yet, in the underdoped regime, the total low-energy spectral weight remains markedly reduced relative to band theory expectations, highlighting the persistence of strong correlation effects across a broad doping range. Effective mass m*, derived from optical and quantum oscillation data, shows logarithmic divergence as p→p*, offering spectroscopic evidence of quantum criticality [35]. Importantly, spectroscopic probes locate the PG endpoint at higher doping (~0.20-0.23) than transport measurements(~0.18-0.19), emphasizing probe-dependent sensitivity rather than contradiction [12, 7].

### 3.0 TEMPERATURE DEPENDENCE OF THE PSEUDOGAP PHASE

#### 3.1 Pseudogap Onset Temperature: Evidence from THG Spectroscopy

The PG onset temperature T*, defines the upper boundary of anomalous electronic behavior distinct from superconductivity [36]. Using terahertz third-harmonic generation (THG) spectroscopy on YBa2Cu3O6+x (YBCO) thin films, [36] observed a nonlinear optical response characterized by the third-order susceptibility, x(3). A distinct signal emerged at TTHG≈ T*, preceding the superconducting transition TC. The temperature-dependent change in slope of x(3) indicates the onset of collective excitations unique to the PG state. Importantly, TTHG values are consistent with polarized neutron scattering and transport results, establishing THG as a sensitive probe of the PG boundary.

These findings align with magnetic susceptibility studies across multiple cuprate families, including La2-xSrxCuO4 ,Bi2Sr2Ca1-xYxCu2O8, and YBa2Cu3O6+y, which show  T* varies linearly with doping and runs tangential to the superconducting dome [37]. This cross-validation between nonlinear optical and magnetic approaches confirms that  T* represents a genuine phase boundary, distinct from Tmax, the antiferromagnetic correlation temperature that transport studies once misattributed as the PG onset [37].

Figure 4: Pseudogap temperature  T* and magnetic correlation temperature Tmax as functions of hole doping for four cuprate families.  T* (Dashed lines) exhibits linear behavior tangential to the superconducting dome (blue curves), while Tmax (solid red lines) decreases linearly up to optimal doping before saturating in the overdoped regime. Data extracted from magnetic susceptibility analysis of (a)  La2-xSrxCuO4, (b) YBa2Cu3O6+y, and (c) Bi2Sr2CaCu2O8+y compounds. The distinction between these temperature scales resolves apparent contradictions between spectroscopic and transport measurements. Adapted from [37].

### 3.2 Nematic Order and Symmetry Breaking

Electronic nematic order characterised by the spontaneous breaking of fourfold rotational C4 symmetry without disrupting translational symmetry, has emerged as a defining hallmark of the PG regime [38, 14]. Resonant X-ray scattering (RXS) measurements in La1.6-xNd0.4SrxCuO4 (Nd-LSCO) demonstrate that nematic order develops below  T*, vanishing abruptly at the critical doping  p*≈0.23, coincident with the disappearance of the PG phase [14, 39]. This sharp boundary suggests that nematicity is not a gradual crossover but a thermodynamic phase transition fundamentally linked to the PG’s origin [38, 14, 39]. Importantly, nematic signatures vary across materials, while Nd-LSCO shows robust anisotropy, YBCO lacks detectable in-plane symmetry breaking [40]. Such contrasts underscore the role of lattice structure, disorder, and competing orders. Theoretical work further proposes nematicity as a vestigial form of charge order, offering a unifying perspective on its persistence across cuprates [41].

## 3.3 Transport and Thermodynamic Signatures of Pseudogap Termination

Transport and thermodynamic measurements provide some of the clearest evidence for the termination of the PG phase and the existence of a quantum critical point (QCP) at p*. Transport consistently reports the lowest critical doping values across cuprate families. In YBCO, quantum oscillations identified  p*=0.18±0.02 [12], while resistivity and Hall measurements in LSCO gave  p*=0.19±0.01 [7]. These values are lower than spectroscopic estimates, reflecting transport’s sensitivity to long-range electronic coherence.

In Nd-LSCO, the in-plane resistivity exhibits distinct scaling: ρT∝T below  T*, transitioning to Fermi-liquid behavior ρT∝T2 beyond the critical point [7]. The coexistence of linear and quadratic terms signals critical scattering near a QCP. Hall effect measurements further reveal abrupt changes in the Hall coefficient at p*, indicating Fermi surface reconstruction [7]. According to [42], the anomalies are interpreted using a phase-separation model in which PG formation produces alternating domains of high and low hole density, with charge density wave (CDW) modulations generating tunneling barriers that govern transport.

Figure 5: Temperature dependence of Hall coefficient RH across the pseudogap regime in La2-xSrxCuO4. Experimental data points from p = 0.01 to p = 0.25 compared with theoretical predictions (continuous lines) from the charge density wave phase separation model. The model successfully reproduces the dramatic temperature variations by considering thermally activated carriers, showing excellent agreement across the pseudogap regime except for p = 0.25 where negative out-of-plane electron contributions emerge above T = 100K. Adapted from [42].

Thermodynamic measurements corroborate these transport signatures. The electronic specific heat coefficient Cel/ T, shows logarithmic divergence as T→0 at p*, consistent with enhanced effective mass and density of states [7, 43]:

CelT=~B lnT0T

Where B quantifies the strength of the divergence and T0 is a reference scale [43]. Similarly, entropy data reveal enhanced Sel/ T at p*, implying that PG collapse liberates electronic states favorable for superconducting pairing [44].

Remarkably, these anomalies coincide with optimal superconductivity: in Eu-LSCO and Nd-LSCO, both Cel/ T and the condensation energy ∆CTC peak at p* [7, 43]. When superconductivity is suppressed by magnetic fields, the normal-state entropy and mass renormalization also maximize at this doping, reinforcing the role of critical fluctuations in pairing.

Quantum oscillations in YBCO confirm effective mass divergence at p* [35], while Hall measurements show a carrier density jump from n=p for p<p* to n=1+p for p>p*, signaling Fermi surface reconstruction [12]. High-field transport in Nd-LSCO demonstrates the universality of these features [45].

Together, transport and thermodynamic evidence strongly support the view that the PG terminates via a sharp quantum phase transition rather than a crossover. At p*, competing orders and superconductivity intersect, defining a universal QCP central to HTSC [7, 43].

#### 3.4 Nature of the Pseudogap Onset: Transition vs. Crossover

A longstanding debate surrounds the PG onset temperature  T* [14, 39]. Does it mark a true phase transition or merely a crossover? Evidence increasingly favors the former. In Nd-LSCO, electronic nematicity vanishes abruptly at  T* [14], with sharp terminations of nematic order also documented in YBCO and Bi-based cuprates. Such abrupt disappearance of symmetry-breaking signatures implies a thermodynamic transition, possibly linked to a QCP at  p* [14, 39]. Complementary evidence arises from nonlinear optical experiments: the THG response in YBCO persists above TC​ and diminishes gradually until vanishing at  T*, reflecting the survival of PG-related collective excitations well above the superconducting state [36]. The persistence and sharp termination of these signals reinforce the interpretation of  T* as a genuine phase boundary rather than a mere crossover.

#### 4.0 DOPING DEPENDENCE OF THE PSEUDOGAP PHASE

4.1 Doping Evolution in Hole vs. Electron-Doped Cuprates

The PG extends across both hole and electron-doped cuprates, though its evolution differs markedly. In hole-doped systems, it emerges as long-range AFM order weakens, persists into the overdoped regime where it coexists with superconductivity, and terminates at a critical doping often identified with a QCP marking a fundamental change in the ground state [46, 33]. In contrast, ARPES studies of Pr1.3-xLa0.7Cex CuO4 (PLCCO) and Nd2-xCexCuO4 (NCCO) reveal that in electron-doped cuprates the PG is largest near the nodal regions and decreases toward the antinodes, the reverse of hole-doped behavior [18]. It persists even after long-range AFM is suppressed, sustained by short-range correlations [47, 45] consistent with CDMFT calculations that attribute its origin to strong local interactions [18]. These contrasting trends underscore both the universality of the PG and its particle–hole asymmetry.

| S/N | Materials | Critical Doping p* | Maximum T*(K) | Primary Method | Key Reference |
| --- | --- | --- | --- | --- | --- |
| 1 | LSCO | 0.19±0.01 | ~150 | Transport/Thermodynamic Measurements | [7] |
| 2 | Nd-LSCO | 0.23±0.01 | ~120 | Transport/RXS | [14] |
| 3 | YBCO | 0.18±0.02 | ~200 | ARPES/Quantum Oscillations | [12] |
| 4 | Bi-2212 | 0.22±0.02 | ~180 | STM/ARPES | [13] |
| 5 | Bi-2201 | 0.21±0.02 | ~160 | STM | [24] |

Table 1: Summary of critical parameters across the cuprate families.

5.0 THEORETICAL FRAMEWORKS OF THE PSEUDOGAP PHASE

Three principal frameworks address PG physics: quantum criticality, strong correlations rooted in Mott physics, and intertwined electronic orders. Rather than being mutually exclusive, each emphasizes complementary aspects of the phenomenon [48, 9].

### 5.1 QUANTUM CRITICALITY FRAMEWORK

The PG endpoint, p*, is widely interpreted as a QCP, where transport, thermodynamic, and magnetic anomalies converge. Distinct non-Fermi liquid scaling, enhanced electronic specific heat, and suppression of AFM correlations all point to quantum critical behavior at p*  [7, 17, 2]. Experimentally, glassy AFM correlations vanish at critical doping [17], the electronic specific heat coefficient dramatically peaks, and resistivity deviates from Fermi-liquid expectations [2]. The collapse of the PG thus coincides with intensified spin fluctuations and thermodynamic anomalies, linking magnetism directly to superconducting optimization [10].

Across multiple cuprate families, the critical doping for these anomalies is strikingly consistent, suggesting a universal quantum critical framework governs PG termination [7, 17]. At the QCP, electronic orders and quasiparticle coherence collapse, separating the PG regime from the Fermi-liquid state.

A unifying perspective is provided by local–itinerant duality: electrons exhibit both localized magnetic moments and itinerant charge character [2]. Spin-fermion and marginal Fermi liquid models capture this duality, reproducing strange-metal transport and effective mass enhancement near p* [49-51]. This framework explains why quasiparticle coherence is reduced while critical fluctuations peak, reinforcing the QCP as central to cuprate physics

5.2 STRONG CORRELATION (MOTT) FRAMEWORK

The PG arises from proximity to a Mott insulating phase, where strong electron interactions lead to fractionalization into spinons and holons, producing momentum-dependent spectral gaps [52, 18]. Cluster DMFT and three-band calculations reproduce correlation-driven spectral weight suppression and in-gap states without long-range order, consistent with ARPES [53-55]. Strong electronic correlations generate momentum and frequency dependent self-energies. Within the Eliashberg framework, electron-boson coupling produces:

k,ω=0∞dΩα2F(k,Ω)ω-Ω+i0++c.c.

For systems with dominant low-energy modes, this reduces to a pole approximation:

k,ω≈gk2ω-Ωk+iΓk+Σimp

Where α2F(k,Ω) represents the electron-boson spectral density, gk2 denotes the momentum-dependent coupling strength, Ωk is the characteristic boson frequency, Γk captures scattering broadening and Σimp accounts for impurity contributions [56-59], This formulation, originally proposed in [56], remains a cornerstone in modern ab initio descriptions of electron–phonon interactions [57].

In the RVB picture, the PG reflects spin-singlet formation in a doped Mott background, with superconductivity emerging from condensation of fractionalized excitations [60-63]. This framework naturally connects to the Uemura relation, where the critical temperature correlates with superfluid density:

TC∝nsm*∝ρs

Establishing that TC is proportional to superfluid density ρs in underdoped cuprates [64-66], reflecting the interplay between spin-gap formation and phase coherence.

5.3 INTERTWINED ORDERS FRAMEWORK

Charge density waves (CDWs) represent a central competing order in the PG regime, breaking translational symmetry throughout underdoped cuprates. Resonant inelastic x-ray scattering (RIXS) in La2-xBaxCuO4  reveals a two-step CDW formation: nearly commensurate precursors at elevated temperatures evolving into incommensurate order upon cooling [31]. Scanning tunneling microscopy (STM) further detects local density of states (LDOS) modulations across broad doping ranges, confirming charge ordering as a robust PG instability.

Pair density waves (PDWs) extend this picture by introducing spatially modulated Cooper pairs that simultaneously break translational and gauge symmetries. These finite-momentum condensates not only frustrate superconducting coherence but also generate associated CDW and magnetic correlations [67, 68]. The PDW order parameter is expressed as:

∆PDWr=∆+eiQ.r+∆-e-iQ.r

Where ∆± represent complex amplitudes for ±Q [68]. Direct STM visualization in Bi2Sr2CaCu2O8+δ uncovered an eight-unit-cell periodic gap modulation (Panel A), the first atomic-scale evidence of spatially modulated Cooper pairs [69]. Fourier analysis resolved PDW wavevectors at Qx=2πa(0.129±0.003, 0) and Qy=2πa(0, 0.118±0.003)  (Panel B) corroborated by particle–hole symmetric gap modulations of ~6 MeV amplitude (Panels C–D). These results firmly establish finite-momentum pairing in cuprates.

FIGURE 6: Atomic-scale visualization of pair-density wave order in Bi2Sr2CaCu2O8+δ.  (A) Energy gap map ∆(r) showing eight-unit-cell periodic modulations with amplitude histogram (inset). (B) Fourier transform revealing PDW peaks at wavevectors Q≈2πa18,0and (0,18). (C) Energy-distance spectroscopy along marked trajectory displaying ~8a0 gap oscillations. (D) Wavevector-resolved profiles confirming PDW peaks at Q=(0.129±0.003, 0) and (0, 0.118±0.003) in units of 2πa0  [69].

Spin density waves (SDWs) further break symmetry and compete with charge orders. Neutron scattering reveals stripe-like correlations up to x=0.26  in Nd-LSCO [70], while ultrasound and complementary probes detects AFM fluctuations persisting to the PG endpoint p* [17], highlighting magnetism’s central role.

A further candidate is loop-current order, invoked to explain time-reversal symmetry breaking. Kerr rotation signals symmetry loss near T* [71], and polarized neutron scattering reports intra-unit-cell magnetic moments [72, 73]. Yet conflicting evidence leaves loop currents debated despite strong theoretical motivation [74].

Together, these intertwined orders define the PG not as a single instability but as a competitive and cooperative landscape. Recent work identifying PDW collective modes [75] and cross-family signatures [76] reinforces this multifaceted framework.

6.0 CONCLUSION

The PG is best regarded as a distinct electronic regime whose endpoint, p*, depends strongly on the probe used, transport locates it at p*≈0.18-0.19 [12], spectroscopy near 0.22 [13], and symmetry-sensitive measurements around 0.23 [14]. Rather than reflecting experimental inconsistency, this hierarchy underscores probe-dependent sensitivity to coherence length and correlation scales. Competing theoretical frameworks, quantum criticality, strong-correlation (Mott/RVB), and intertwined orders each capture complementary aspects of these findings, converging on a picture of multifaceted electronic reconstruction at the PG endpoint [9, 18, 31]. Notably, the coincidence of transport-determined p* with optimal TC highlights that restoring long-range coherence, rather than fully eliminating local PG signatures, is key to maximizing superconductivity. Addressing the remaining discrepancies demands systematic cross-technique studies on identical crystals and correlation-length–resolved probes to test whether these offsets are intrinsic.

### 7.0 FUTURE DIRECTIONS AND OPEN CHALLENGES

Systematic differences in PG critical doping require careful validation, transport places p*≈0.18-0.19 [12], spectroscopy near 0.22  [13], and symmetry probes at 0.23  [14]. Whether these offsets reflect intrinsic physics or sample preparation artifacts can only be resolved through cross-technique studies on identical crystals. Probing correlation-length effects by tuning temperature, disorder, and magnetic field offers a promising strategy, as transport and spectroscopic probes may access different spatial scales of electronic reconstruction. On the theoretical front, [9] explains the transport anomalies; [18] interprets spectroscopic features, and intertwined-order models capture symmetry breaking [31, 24]. Whether these frameworks converge on a unified picture remains unresolved. Crucially, the alignment of transport-defined p* with optimal TC [7, 8] underscores that superconducting optimization hinges on restoring coherence rather than fully erasing PG signatures.

Disclaimer (Artificial intelligence):

Author(s) hereby declare that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc.) and text-to-image generators have been used during the writing or editing of this manuscript.

REFERENCES:

- Bandur, D., Nachtigal, J., Tsankov, S., Lee, A. J., & Haase, J. (2023). Cuprate universal electronic spin response and the pseudogap from NMR. https://doi.org/10.48550/arxiv.2309.11874

- Li, T. (2021). A short review of the recent progresses in the study of the cuprate superconductivity. Chinese Physics B, 30(10), 100508. https://doi.org/10.1088/1674-1056/ABFA04

- Bacq-Labreuil, B., Lacasse, B., Tremblay, A. –M. S., Sénéchal, D., & Haule, K. (2024). Towards an ab initio theory of high-temperature superconductors: a study of multilayer cuprates. https://doi.org/10.48550/arxiv.2410.10019

- Niu, J., Ortego Larrazabal, M., Gozlinski, T., Sato, Y., Bastiaans, K. M., Benschop, T., Ge, J.-F., Blanter, Y. M., Gu, G., Swart, I., & Allan, M. P. (2024). Equivalence of pseudogap and pairing energy in a cuprate high-temperature superconductor. https://doi.org/10.48550/arxiv.2409.15928

- Boschini, F., Zonno, M., Razzoli, E., Day, R., Michiardi, M., Michiardi, M., Zwartsenberg, B., Nigge, P., Schneider, M., da Silva Neto, E. H., Erb, A., Zhdanovich, S., Mills, A. K., Levy, G., Giannetti, C., Jones, D. J., & Damascelli, A. (2020). Emergence of pseudogap from short-range spin-correlations in electron-doped cuprates. 5(1), 1–7. https://doi.org/10.1038/S41535-020-0208-6

- Julià-Farré, S., Dauphin, A., Chhajlany, R. W., Grochowski, P. T., Wall, S., Lewenstein, M., Grzybowski, P. R., & Grzybowski, P. R. (2020). Nanoscale phase separation and pseudogap in the hole-doped cuprates from fluctuating Cu-O-Cu bonds. Physical Review B, 101(12), 125107. https://doi.org/10.1103/PHYSREVB.101.125107

- Michon, B., Girod, C., Girod, C., Girod, C., Badoux, S., Kacmarcik, J., Ma, Q., Dragomir, M., Dabkowska, H., Gaulin, B. D., Gaulin, B. D., Zhou, J.-S., Pyon, S., Takayama, T., Takagi, H., Verret, S., Doiron-Leyraud, N., Marcenat, C., Taillefer, L., … Klein, T. (2019). Thermodynamic signatures of quantum criticality in cuprate superconductors. Nature, 567(7747), 218–222. https://doi.org/10.1038/S41586-019-0932-X

- Legros, A., Legros, A., Benhabib, S., Tabis, W., Tabis, W., Laliberte, F., Dion, M., Lizaire, M., Vignolle, B., Vignolles, D., Raffy, H., Li, Z., Auban-Senzier, P., Doiron-Leyraud, N., Fournier, P., Fournier, P., Colson, D., Taillefer, L., Taillefer, L., … Proust, C. (2019). Universal T -linear resistivity and Planckian dissipation in overdoped cuprates. Nature Physics, 15(2), 142–147. https://doi.org/10.1038/S41567-018-0334-2

- Yang, J., & Li, T. (2024). A tale of two pairs: on the origin of the pseudogap end point in the high-T$_{c}$ cuprate superconductors. https://doi.org/10.48550/arxiv.2402.02785

- Zhu, M., Voneshen, D. J., Raymond, S., Lipscombe, O. J., Tam, C. C., & Hayden, S. M. (2022). Spin fluctuations associated with the collapse of the pseudogap in a cuprate superconductor. Nature Physics, 19(1), 99–105. https://doi.org/10.1038/s41567-022-01825-3

- Taillefer, L. (2010). Scattering and Pairing in Cuprate Superconductors. Annual Review of Condensed Matter Physics, 1(1), 51–70. https://doi.org/10.1146/ANNUREV-CONMATPHYS-070909-104117

- Badoux, S., Tabis, W., Laliberte, F., Grissonnanche, G., Vignolle, B., Vignolles, D., Béard, J., Bonn, D. A., Hardy, W., Liang, R., Doiron-Leyraud, N., Taillefer, L., & Proust, C. (2016). Change of carrier density at the pseudogap critical point of a cuprate superconductor. Nature, 531(7593), 210–214. https://doi.org/10.1038/NATURE16983

- Loret, B., Gallais, Y., Cazayous, M., Zhong, R., Schneeloch, J., Gu, G., Fedorov, A. V., Kim, T. K., Borisenko, S. V., & Sacuto, A. (2018). Raman and ARPES combined study on the connection between the existence of the pseudogap and the topology of the Fermi surface in Bi 2 Sr 2 CaCu 2 O 8 + δ. Physical Review B, 97(17), 174521. https://doi.org/10.1103/PHYSREVB.97.174521

- Gupta, N. K., McMahon, C., Sutarto, R., Shi, T., Gong, R., Wei, H. I., Shen, K., He, F., Ma, Q., Dragomir, M., Gaulin, B. D., Gaulin, B. D., & Hawthorn, D. (2021). Vanishing nematic order beyond the pseudogap phase in overdoped cuprate superconductors. Proceedings of the National Academy of Sciences of the United States of America, 118(34), 2106881118. https://doi.org/10.1073/PNAS.2106881118

- Tallon, J. L., & Loram, J. (2001). The doping dependence of T* – what is the real high-Tc phase diagram? Physica C-Superconductivity and Its Applications, 349(1), 53–68. https://doi.org/10.1016/S0921-4534(00)01524-0

- Cyr-Choinière, O., Daou, R., Laliberte, F., Collignon, C., Badoux, S., LeBoeuf, D., Juul Chang, J., Ramshaw, B., Bonn, D. A., Bonn, D. A., Hardy, W., Hardy, W., Liang, R., Liang, R., Yan, J., Cheng, J. G., Zhou, J.-S., Goodenough, J. B., Pyon, S., … Taillefer, L. (2018). Pseudogap temperature T* of cuprate superconductors from the Nernst effect. Physical Review B, 97(6), 064502. https://doi.org/10.1103/PHYSREVB.97.064502

- Frachet, M., Vinograd, I., Zhou, R., Benhabib, S., Wu, S. F., Mayaffre, H., Krämer, S., Ramakrishna, S. K., Reyes, A. P., Debray, J., Kurosawa, T., Momono, N., Oda, M., Komiya, S., Ono, S., Horio, M., Chang, J., Proust, C., Leboeuf, D., & Julien, M.-H. (2019). Hidden magnetism at the pseudogap critical point of a high temperature superconductor. arXiv: Superconductivity. https://doi.org/10.1038/S41567-020-0950-5

- Horio, M., Sakai, S., Suzuki, H., Nonaka, Y., Hashimoto, M., Lu, D.-H., Shen, Z., Ohgi, T., Konno, T., Adachi, T., Koike, Y., Imada, M., & Fujimori, A. (2024). Pseudogap in electron-doped cuprates: Strong correlation leading to band splitting. Proceedings of the National Academy of Sciences of the United States of America, 122(1). https://doi.org/10.1073/pnas.2406624122

- Vilk, Y. M., Lahaie, C., & Tremblay, A.-M. S. (2024). Antiferromagnetic pseudogap in the two-dimensional Hubbard model deep in the renormalized classical regime. Physical Review. https://doi.org/10.1103/physrevb.110.125154

- Gauvin-Ndiaye, C., LaHaie, C. B., Vilk, Y. M., & Tremblay, A.-M. (2023). Improved two-particle self-consistent approach for the single-band Hubbard model in two dimensions. Physical Review. https://doi.org/10.1103/physrevb.108.075144

- Hashimoto, M., Vishik, I., He, R., Devereaux, T. P., Devereaux, T. P., Shen, Z.-X., Shen, Z.-X., & Shen, Z.-X. (2014). Energy gaps in high-transition-temperature cuprate superconductors. Nature Physics, 10(7), 483–495. https://doi.org/10.1038/NPHYS3009

- Yoshida, T., Hashimoto, M., Vishik, I., Shen, Z.-X., & Fujimori, A. (2012). Pseudogap, Superconducting Gap, and Fermi Arc in High-Tc Cuprates Revealed by Angle-Resolved Photoemission Spectroscopy. Journal of the Physical Society of Japan, 81(1), 011006. https://doi.org/10.1143/JPSJ.81.011006

- Doronkina, S. V., Myasnikova, A. E., Dzhantemirov, A. H., & Lutsenko, A. V. (2022). Topological pseudogap in highly polarizable layered systems with 2D hole-like dispersion. Physica E-Low-Dimensional Systems & Nanostructures, 136, 115052. https://doi.org/10.1016/J.PHYSE.2021.115052

- Fei, Y., Zheng, Y., Bu, K., Zhang, W., Ding, Y., Zhou, X., Yin, Y., & Yin, Y. (2019). Visualizing the charge order and topological defects in an overdoped (Bi,Pb)$_2$Sr$_2$CuO$_{6+x}$ superconductor. arXiv: Superconductivity. https://doi.org/10.1007/S11433-019-9454-6

- Neto, E. H. da S., Frañó, A., & Boschini, F. (2024). Dynamic charge order from strong correlations in the cuprates. Frontiers in Electronic Materials, 4. https://doi.org/10.3389/femat.2024.1473324

- Hoffman, J., Hudson, E., Lang, K., Madhavan, V., Eisaki, H., Uchida, S., & Davis, J. C. (2002). A Four Unit Cell Periodic Pattern of Quasi-Particle States Surrounding Vortex Cores in Bi2Sr2CaCu2O8+δ. ChemInform, 33(15). https://doi.org/10.1002/CHIN.200215010

- Mukhopadhyay, S., Mukhopadhyay, S., Sharma, R., Sharma, R., Kim, C. K., Edkins, S. D., Hamidian, M., Eisaki, H., Uchida, S., Kim, E.-A., Lawler, M. J., Mackenzie, A. P., Davis, J. C. S., Davis, J. C. S., & Fujita, K. (2019). Evidence for a vestigial nematic state in the cuprate pseudogap phase. Proceedings of the National Academy of Sciences of the United States of America, 116(27), 13249–13254. https://doi.org/10.1073/PNAS.1821454116

- Avramovska, M., Nachtigal, J., & Haase, J. (2022). $$^{17}$$O and $$^{89}$$Y NMR Shift and Relaxation and the Temperature-Independent Pseudogap of the Cuprates. Journal of Superconductivity and Novel Magnetism. https://doi.org/10.1007/s10948-022-06171-2

- Tahir‐Kheli, J. (2024). Evidence for Atomic-Scale Inhomogeneity in Superconducting Cuprate NMR. https://doi.org/10.48550/arxiv.2411.08142

- Arpaia, R., & Ghiringhelli, G. (2021). Charge order at high temperature in cuprate superconductors. Journal of the Physical Society of Japan, 90(11), 111005. https://doi.org/10.7566/JPSJ.90.111005

- Miao, H., Fumagalli, R., Rossi, M. A. C., Lorenzana, J., Seibold, G., Yakhou-Harris, F., Kummer, K., Brookes, N. B., Gu, G. D., Braicovich, L., Ghiringhelli, G. C., & Dean, M. (2019). Formation of Incommensurate Charge Density Waves in Cuprates. arXiv: Superconductivity. https://doi.org/10.1103/PHYSREVX.9.031042

- Mitsen, K., & Ivanenko, O. M. (2024). On the physical nature of pseudogap phase and anomalous transfer of spectral weight in underdoped cuprates. https://doi.org/10.48550/arxiv.2401.12647

- Michon, B., Kuzmenko, A. B., Tran, M. K., McElfresh, B., Komiya, S., Ono, S., Uchida, S., & van der Marel, D. (2021). The spectral weight of hole doped cuprates across the pseudogap critical point. arXiv: Superconductivity. http://export.arxiv.org/pdf/2110.06563

- Basov, D., & Timusk, T. (2005). Electrodynamics of high- T c superconductors. Reviews of Modern Physics, 77(2), 721–779. https://doi.org/10.1103/REVMODPHYS.77.721

- Ramshaw, B., Sebastian, S. E., McDonald, R. D., Day, J., Tan, B. S., Zhu, Z., Betts, J. B., Liang, R., Bonn, D. A., Bonn, D. A., Hardy, W. N., Hardy, W. N., & Harrison, N. (2015). Quasiparticle mass enhancement approaching optimal doping in a high-Tc superconductor. Science, 348(6232), 317–320. https://doi.org/10.1126/SCIENCE.AAA4990

- Yuan, J., Shi, L., Yue, L., Li, B., Wang, Z., Xu, S., Xu, T.-Q., Wang, Y., Gan, Z., Chen, F., Lin, Z., Wang, X., Jin, K., Wang, X., Luo, J., Zhang, S., Wu, Q., Liu, Q., Hu, T., … Wang, N. (2024). Dynamical interplay between superconductivity and pseudogap in cuprates as revealed by terahertz third-harmonic generation spectroscopy. Science Advances, 10. https://doi.org/10.1126/sciadv.adg9211

- Noat, Y., Mauger, A., Nohara, M., Eisaki, H., Ishida, S., & Sacks, W. (2022). Cuprates phase diagram deduced from magnetic susceptibility: What is the ‘true’ pseudogap line? Solid State Communications, 348–349, 114689. https://doi.org/10.1016/j.ssc.2022.114689

- Hawthorn, D. (2023). Resonant X-Ray Scattering Investigations of Charge Density Wave and Nematic Orders in Cuprate Superconductors. Synchrotron Radiation News, 36, 9–15. https://doi.org/10.1080/08940886.2023.2224733

- Sato, Y., Kasahara, S., Murayama, H., Kasahara, Y., Moon, E.-G., Nishizaki, T., Loew, T., Porras, J., Keimer, B., Shibauchi, T., & Matsuda, Y. (2017). Thermodynamic evidence for a nematic phase transition at the onset of the pseudogap in YBa 2 Cu 3 O y. Nature Physics, 13(11), 1074–1078. https://doi.org/10.1038/NPHYS4205

- Grissonnanche, G., Cyr-Choinière, O., Day, J., Liang, Rx., Bonn, D. A., Hardy, W. N., Doiron-Leyraud, N., & Taillefer, L. (2022). No nematicity at the onset temperature of the pseudogap phase in the cuprate superconductor YBCO.

- Kivelson, S. A., & Lederer, S. (2019). Linking the pseudogap in the cuprates with local symmetry breaking: A commentary. Proceedings of the National Academy of Sciences of the United States of America, 116(29), 14395–14397. https://doi.org/10.1073/PNAS.1908786116

- Anjos, J. C., Santana, H., & de Mello, E. V. L. (2024). The role of the pseudogap in cuprate superconductors revealed by the Hall effect. https://doi.org/10.48550/arxiv.2401.05213

- Girod, C., Girod, C., LeBoeuf, D., Demuer, A., Seyfarth, G., Imajo, S., Kindo, K., Kohama, Y., Lizaire, M., Legros, A., Gourgout, A., Takagi, H., Kurosawa, T., Oda, M., Momono, N., Chang, J., Ono, S., Zheng, G.-Q., Zheng, G.-Q., … Klein, T. (2021). Normal state specific heat in the cuprate superconductors La 2 − x Sr x CuO 4 and Bi 2 + y Sr 2 − x − y La x CuO 6 + δ near the critical point of the pseudogap phase. Physical Review B, 103(21), 214506. https://doi.org/10.1103/PHYSREVB.103.214506

- Tallon, J. L., Storey, J., Cooper, J. R., & Loram, J. (2020). Locating the pseudogap closing point in cuprate superconductors: Absence of entrant or reentrant behavior. Physical Review B, 101(17), 174512. https://doi.org/10.1103/PHYSREVB.101.174512

- Collignon, C., Collignon, C., Badoux, S., Afshar, S. A. A., Michon, B., Laliberte, F., Cyr-Choinière, O., Zhou, J.-S., Licciardello, S., Wiedmann, S., Doiron-Leyraud, N., Taillefer, L., & Taillefer, L. (2017). Fermi-surface transformation across the pseudogap critical point of the cuprate superconductor La1.6-xNd0.4SrxCuO4. Physical Review B, 95(22), 224517. https://doi.org/10.1103/PHYSREVB.95.224517

- Lizaire, M., Legros, A., Legros, A., Gourgout, A., Benhabib, S., Badoux, S., Laliberte, F., Boulanger, M.-E., Ataei, A., Grissonnanche, G., Leboeuf, D., Licciardello, S., Wiedmann, S., Ono, S., Raffy, H., Kawasaki, S., Zheng, G.-Q., Zheng, G.-Q., Doiron-Leyraud, N., … Taillefer, L. (2021). Transport signatures of the pseudogap critical point in the cuprate superconductor Bi 2 Sr 2 − x La x CuO 6 + δ. Physical Review B, 104(1), 014515. https://doi.org/10.1103/PHYSREVB.104.014515

- Miyamoto, M., Horio, M., Moriya, K., Takahashi, A., Osiecki, J., Balasubramanian, T., Polley, C., Koike, Y., Adachi, T., Mizokawa, T., & Matsuda, I. (2024). Inhomogeneous reduction-annealing effects on the electron-doped cuprate superconductor revealed by micro-focused angle-resolved photoemission spectroscopy. https://doi.org/10.48550/arxiv.2412.04790

- Keimer, B., Moore, J. E., & Moore, J. E. (2017). The physics of quantum materials. Nature Physics, 13(11), 1045–1055. https://doi.org/10.1038/NPHYS4302

- Wu, W., Wang, X., & Tremblay, A.-M. (2021). Non-Fermi liquid phase and linear-in-temperature scattering rate in overdoped two-dimensional Hubbard model. (2022). Proceedings of the National Academy of Sciences, 119(13). https://doi.org/10.1073/pnas.2115819119

- Zhang, Y.-H., & Sachdev, S. (2020). From the pseudogap metal to the Fermi liquid using ancilla qubits. arXiv: Strongly Correlated Electrons. https://doi.org/10.1103/PHYSREVRESEARCH.2.023172

- Patel, A. A., Guo, H., Esterlis, I., & Sachdev, S. (2023). Universal theory of strange metals from spatially random interactions. Science, 381(6659), 790–793. https://doi.org/10.1126/science.abq6011

- Lee, P. A., Nagaosa, N., & Wen, X.-G. (2004). Doping a Mott Insulator: Physics of High Temperature Superconductivity. arXiv: Strongly Correlated Electrons. http://ui.adsabs.harvard.edu/abs/2004cond.mat.10445L/abstract

- Sordi, G., Semon, P., Haule, K., Tremblay, A.-M., & Tremblay, A.-M. (2012). Strong Coupling Superconductivity, Pseudogap, and Mott Transition. Physical Review Letters, 108(21), 216401. https://doi.org/10.1103/PHYSREVLETT.108.216401

- Mai, P., Balduzzi, G., Johnston, S., & Maier, T. (2021). Pairing correlations in the cuprates: A numerical study of the three-band Hubbard model. Physical Review B, 103(14), 144514. https://doi.org/10.1103/PHYSREVB.103.144514

- Cassol, F., Gaspard, L., Casula, M., Martins, C., & Lenz, B. (2024). Rich phase diagram of the prototypical iridate Ba2IrO4: Effective low-energy models and metal-insul. Physical Review. https://doi.org/10.1103/physrevb.109.155120

- Engelsberg, S., & Schrieffer, J. R. (1963). Coupled Electron-Phonon System. Physical Review, 131(3), 993–1008. https://doi.org/10.1103/PHYSREV.131.993

- Giustino, F. (2017). Electron-phonon interactions from first principles. Reviews of Modern Physics, 89(1), 015003. https://doi.org/10.1103/REVMODPHYS.89.015003

- Mahan, G. D. (2000). Many-particle physics (3rd ed.). Springer, New York. ISBN 978-1-4419-3339-3. https://doi.org/10.1007/978-1-4757-5714-9

- Park, H., Park, J. H., & Hwang, J. (2021). Electron-boson Spectral Density Functions of Cuprates Obtained from Optical Spectra Via Machine Learning. https://doi.org/10.1103/physrevb.104.235154

- Leon, D. A., Berland, K., & Cardoso, C. (2025). Spectral properties from an efficient analytical representation of the $GW$ self-energy within a multipole approximation. https://doi.org/10.48550/arxiv.2501.09121

- Zhang, C., & Li, T. (2020). Resonating valence bond theory of anomalous spin dynamics of spin-1/2 triangular lattice Heisenberg antiferromagnet and its application to Ba 3 CoSb 2 O 9. Physical Review B, 102(7), 075108. https://doi.org/10.1103/PHYSREVB.102.075108

- Singh, N. (2022). Is the problem of Cuprate high-$ T_c $ superconductivity a solved problem?. arXiv preprint arXiv:2211.00400.

- Song, Z., Zhang, J., & Weng, Z.-Y. (2024). Thermal Hall effect and neutral spinons in a doped Mott insulator. Physical Review Research, 6(2). https://doi.org/10.1103/physrevresearch.6.023328

- Uemura, Y. J., Luke, G., Sternlieb, B. J., Brewer, J. H., Carolan, J. F., Hardy, W., Kadono, R., Kempton, J. R., Kiefl, R. F., Kreitzman, S. R., Mulhern, P., Riseman, T. M., Williams, D., Yang, B. X., Uchida, S., Takagi, H., Gopalakrishnan, J., Sleight, A. W., Subramanian, M. A., … Yu, X. H. (1989). Universal correlations between Tc and ns/m (carrier density over effective mass) in high-Tc cuprate superconductors. Physical Review Letters, 62(19), 2317–2320. https://doi.org/10.1103/PHYSREVLETT.62.2317

- Božović, I., He, X., He, X., Wu, J., & Bollinger, A. (2016). Dependence of the critical temperature in overdoped copper oxides on superfluid density. Nature, 536(7616), 309–311. https://doi.org/10.1038/NATURE19061

- Zhao, J., Cai, S., Chen, Y., Gu, G., Yan, H., Guo, J., Han, J., Wang, P., Zhou, Y., Li, Y., Li, X., Ren, Z., Wu, Q., Zhou, X., Ding, Y., Xiang, T., Mao, H., & Sun, L. (2024). Evolution of superconducting-transition-temperature with superfluid density and conductivity in pressurized cuprate superconductors. Chinese Physics Letters. https://doi.org/10.1088/0256-307x/41/4/047401

- Dai, Z., Senthil, T., & Lee, P. A. (2020). Modeling the pseudogap metallic state in cuprates: Quantum disordered pair density wave. Physical Review B, 101(6), 064502. https://doi.org/10.1103/PHYSREVB.101.064502

- Agterberg, D. F., Davis, J. C. S., Davis, J. C. S., Edkins, S. D., Fradkin, E., Van Harlingen, D. J., Kivelson, S. A., Lee, P. A., Radzihovsky, L., Tranquada, J. M., & Wang, Y. (2020). The Physics of Pair-Density Waves: Cuprate Superconductors and Beyond. Annual Review of Condensed Matter Physics, 11(1), 231–270. https://doi.org/10.1146/ANNUREV-CONMATPHYS-031119-050711

- Du, Z., Li, H., Li, H., Joo, S. H., Donoway, E. P., Donoway, E. P., Lee, J., Davis, J. C. S., Davis, J. C. S., Gu, G., Johnson, P. D., & Fujita, K. (2020). Imaging the energy gap modulations of the cuprate pair-density-wave state. Nature, 580(7801), 65–70. https://doi.org/10.1038/S41586-020-2143-X

- Ma, Q., Smith, E. M., Cronkwright, Z. W., Dragomir, M., Mitchell, G., Kolesnikov, V. I., Stone, M. B., & Gaulin, B. D. (2022). Dynamic parallel spin stripes from the 1/8 anomaly to the end of superconductivity in La1.6−x. Physical Review Research, 4(1). https://doi.org/10.1103/physrevresearch.4.013175

- Xia, J., Xia, J., Schemm, E., Schemm, E., Deutscher, G., Kivelson, S. A., Kivelson, S. A., Bonn, D. A., Hardy, W., Liang, R., Siemons, W., Siemons, W., Koster, G., Koster, G., Fejer, M. M., Kapitulnik, A., & Kapitulnik, A. (2008). Polar Kerr-effect measurements of the high-temperature YBa2Cu3O6+x superconductor: evidence for broken symmetry near the pseudogap temperature. Physical Review Letters, 100(12), 127002. https://doi.org/10.1103/PHYSREVLETT.100.127002

- Fauqué, B., Sidis, Y., Hinkov, V., Pailhès, S., Pailhès, S., Lin, C., Chaud, X., & Bourges, Ph. (2006). Magnetic Order in the Pseudogap Phase of High- T C Superconductors. Physical Review Letters, 96(19), 197001. https://doi.org/10.1103/PHYSREVLETT.96.197001

- Li, Y., Balédent, V., Barišić, N., Barišić, N., Cho, Y., Cho, Y., Fauqué, B., Sidis, Y., Yu, G., Zhao, X., Zhao, X., Bourges, P., & Greven, M. (2008). Unusual magnetic order in the pseudogap region of the superconductor HgBa2CuO4+δ. Nature, 455(7211), 372–375. https://doi.org/10.1038/NATURE07251

- Varma, C. (2020). Thermal Hall effect in the pseudogap phase of cuprates. Physical Review B, 102(7), 075113. https://doi.org/10.1103/PHYSREVB.102.075113

- Wu, Y., Chubukov, A. V., Wang, Y., & Kivelson, S. A. (2025). Time-reversal symmetry breaking, collective modes, and Raman spectrum in pair-density-wave states. Npj Quantum Materials, 10(1). https://doi.org/10.1038/s41535-025-00808-w

- Lee, J., Kivelson, S., Wang, T., Ikeda, Y., Taniguchi, T., Fujita, M., & Kao, C. ‐C. (2023). Pair-density wave signature observed by x-ray scattering in La-based high-Tc cuprates. https://doi.org/10.21203/rs.3.rs-3514922/v1