Original Research Article

Numerical Analysis of the Fatigue of Steel Fiber Reinforced Concrete Beams Using Using ANSYS Workbench Simulation

# Abstract

Aims: The primary aim of this study was to evaluate the fatigue behavior of Steel Fiber Reinforced Concrete (SFRC) beams subjected to cyclic loading. Specifically, this study investigates the influence of fiber content on the fatigue performance of concrete beams using numerical simulations in ANSYS Workbench.

Study Design: The study employed a computational approach using the Finite Element Method (FEM) to model SFRC beams with varying fiber contents. The models were analyzed under cyclic loading conditions to assess the fatigue life and stress distribution across the beams.

Methodology: Three finite element models of steel fiber–reinforced concrete (SFRC) beams were simulated, corresponding to steel fiber volume fractions of 0.0% (plain concrete), 1.0%, and 1.5%. The analyses were performed in ANSYS Workbench, where the concrete matrix was modeled using SOLID186 elements, and the steel fibers were represented by LINK180 elements embedded within the beam volume. A zero-based cyclic four-point bending load corresponding to 60% of the static ultimate load was applied, with supports and loading points defined as simple supports and concentrated loads, respectively.

Fatigue life assessment was conducted using the S–N curve approach for both materials, combined with the Goodman mean-stress correction to account for multiaxial stress effects. The fatigue tool in ANSYS was used to evaluate stress distribution, damage progression, and fatigue sensitivity for each fiber content case.

Results: The results showed that increasing the fiber content improved the fatigue life and delayed failure. The model with 1.0% fiber content demonstrated the best balance between durability and numerical stability, while higher fiber content (1.5%) resulted in a marginally higher fatigue safety factor but increased computational instability. Specifically, the fatigue safety factor (FS) increased from 50.6% for plain concrete to 53.1% for 1.0% fiber and 56.6% for 1.5% fiber, representing an enhancement of up to 6.0 percentage points. The predicted fatigue life for all models remained within the range of 10⁶ cycles, However, the presence of fibers resulted in a slower stiffness degradation rate and a reduction in maximum cyclic deflection of approximately 12–15% compared to the control beam.

Conclusion: The study confirms the beneficial role of steel fibers in improving the fatigue performance of concrete beams. These findings highlight the importance of optimizing fiber dosage in the structural design of SFRC elements to achieve greater service life and resilience under cyclic loading. The outcomes can guide performance-based design strategies and material selection in infrastructure exposed to repeated stress conditions, promoting more durable and sustainable concrete structures.

Keywords: Concrete, Steel fibers, Finite element, SFRC, Fatigue behavior.

# INTRODUCTION

Concrete is one of the world's most widely used building materials due to its strength, durability, and low cost [1]. However, it has a significant limitation, its low tensile strength, which makes it susceptible to cracking and structural failure under repeated stresses [2].

In this context, Fiber-Reinforced Concrete (FRC) has emerged as an effective solution to improve the mechanical properties of concrete, especially concerning its fatigue resistance, a critical factor in structures subjected to cyclic loading, such as road pavements, bridges and runways [3].

Steel fiber reinforced concrete (SFRC) has proven to be particularly effective due to the high strength of the steel fibers, which provide localized reinforcement that limits crack propagation and improves the energy absorption capacity of the material. [4]. Steel fibers also improve the ductility of concrete, allowing it to withstand greater deformation before failure [5].

Despite its advantages, the fatigue behavior of SFRC remains an underexplored area, especially when it comes to the interaction between the metallic fibers and the concrete matrix under repetitive loading [6].

The analysis of the behavior of SFRC under fatigue conditions is fundamental to understanding its long-term performance in structures subjected to cyclic loading. However, due to the complexity of the mechanisms involved and the random interaction of the fibers, experimental studies can be costly and limited [7].

In this sense, the use of the Finite Element Method (FEM) is presented as a tool to model and simulate the behavior of the SFRC, allowing the study of its performance without the costs and limitations of physical tests [8].

FEM is a technique widely used in structural engineering that allows simulating the interaction between the steel fiber and the concrete matrix, taking into account the random orientation and distribution of the fibers in the material. This approach is beneficial for the design of structures that will use SFRC, as it provides a detailed analysis of how these factors influence the fatigue strength of the concrete[9].

Through detailed simulations, meaningful results can be obtained contributing to the design of more durable and safer structures, adapted to the specific conditions of each project.

In addition, the implementation of computational models in ANSYS using the Ansys Parametric Design Language (APDL) has allowed for greater practicality in the representation of the SFRC, facilitating the integration of the properties of concrete and steel fibers [10].

Numerical simulations provide a solid basis for experimental validation and allow the improvement of specifications for the use of SFRC in the construction industry. Thus, progress is made in the development of standards and methodologies that can be adopted in infrastructure design, reducing the risk of structural failure and improving the long-term durability of structures [11].

# Methodology

## Development of the Computational Model in ANSYS APDL

The methodology was structured in a sequence of phases that included the development of the model in ANSYS APDL, its subsequent import into Workbench, the setup of the structural and fatigue analysis, and finally the simulation. A computational approach was employed to simulate the four-point bending test in steel fiber reinforced concrete (SFRC), incorporating cyclic loads evaluated using Workbench's Fatigue Tool. The general workflow is shown in the Fig. 1.

Definition of geometric and material properties

Geometry and mesh generation in ANSYS APDL

Random distribution of fibers

Application of boundary conditions and loads

Import to ANSYS Workbench

Structural analysis configuration and Fatigue Tool

Simulation and analysis of results

Fig. 1 Flow chart

### Definition of Geometric Properties

First, the geometric dimensions of the SFRC beam and steel fibers were defined using parameters in the APDL code. The beam was modeled as a rectangular prism with a base (B) of 15 cm, height (H) of 15 cm, and a total length (LAR) of 70 cm, with a free span between supports of 60 cm. These dimensions were based on previous experimental tests to ensure comparability [12].

The steel fibers were parameterized with a diameter (DN) of 0.055 cm (0.55 mm), length (LN) of 3.5 cm, and an initial volumetric content (PF) that could be adjusted by performing simulations, calculating the number of elements generated to represent them as shown in (1), where.

| NFI=Vbl*0.01*PFVFI | (1) |
| --- | --- |

Where:

NFI= ​ Total number of fibers generated

Vbl=  Total beam volume

PF= Volumetric fiber content

VFI= Unit volume of a fiber

Based on this ratio, the total number of fibers is determined by considering the beam volume and the volumetric content, adjusted to the unit volume of each fiber. The specific values for these properties are presented in Table. 1.

Table. 1. Properties of steel fibers

| Property | Value |
| --- | --- |
| % Volumetric (Vf) | 0.5 % |
| Diameter | 0.55 mm |
| Long | 35.0 mm |
| Aspect ratio (lf/ld) | 65 |
| Modulus of Elasticity | 2,100.00 kg/cm² |
| Poisson Module | 0.30 |
| Morphology | Round |

Distances for supports and loads were established: the distance between supports is 5 cm from the ends, and 10 cm for load application points, simulating the four-point bending test. These parameters are summarized in Table. 2.

Table. 2. Properties of the concrete beam

| Property | Value |
| --- | --- |
| Section Type | Rectangular |
| Base (cm) | 15 cm |
| Height (cm) | 15 cm |
| Overall Length (cm) | 70 cm |
| Free span between supports (cm) | 60 cm |
| Compressive strength (kg/cm²) | 275 kg/cm² |
| Poisson Module | 0.1 |
| Volumetric weight (kg/m³) | 2400 kg/m³ |

These properties were assigned in ANSYS Workbench, using the integrated catalog for concrete and structural steel, with the addition of S-N curves for fatigue analysis.

### Geometry and Mesh Generation

Subsequently, the geometry of the beam and its mesh were generated in MECHANICAL APDL. The geometry was created as a rectangular block, as shown in Fig. 2, defining the previously established dimensions (base of 15 cm, height of 15 cm, and length of 70 cm).

Fig. 2. Specimen geometry and support conditions

The mesh was generated by selecting finite elements suitable for concrete and fibers. The SOLID186 element was used, which is a three-dimensional element with the option of 20 or 10nodes, suitable for volumetric solids, Fig. 3. a), At the same time, the fibers were modeled with LINK180, a one-dimensional element of 2 nodes, Fig. 3. b). The mesh size was controlled with the parameter as a function of integer divisions of the base dimension, and iteratively refined, if necessary, until a sufficient number of nodes was reached for adequate fiber distribution.

a)

b)

Fig. 3. Finite elements implemented in the simulation

### Random Distribution of Steel Fibers

The random distribution of steel fibers within the SFRC beam was implemented in ANSYS APDL using a stochastic algorithm. The process started by calculating the fiber number as a function of the volumetric content (PF), using  (1)

The finite element model of the beam contains a set of Nnodes, each with coordinates xi=(xi,yi,zi), where i=1,2,…,Nnodes. For each fiber, an initial node is randomly selected from among these nodes. This process uses a discrete uniform distribution over the interval 1,2,…,Nnodes.

The orientation of each fiber was defined in a complex coordinate system centered at xi. The fiber direction was established by a random rotation in three-dimensional space, parameterized by three angles α,β,γ, representing rotations around the x,y ,and z axes respectively. Each angle was taken independently, using a uniform distribution at [0,360°]:

| α,β,γ~U(0,360) | (2) |
| --- | --- |

In the local coordinate system, the end node of the fiber is initially defined in the x-axis direction with a distance equal to the fiber length, i.e.,x_x2'=(l,0,0). This vector is transformed to the global system by applying a rotation and translating it to the initial node:

| x2=x1+R∙x2' | (3) |
| --- | --- |

It is not explicitly verified whether x_2 is within the limits of the beam. (0,B×0,H×0,L), but the selection of initial nodes within the volume and the relatively short length of fibers (l=3.5 cm frente a L=70 cm) minimize the likelihood that x2 fall out.

Each fiber was represented as a linear element connecting x1 and x2. The element length, le=x2-x1, is calculated as follows:

| le=x2+x12+y2+y12+z2+z12 | (4) |
| --- | --- |

If le≈0, this element is discarded. If le≈l, the fiber is considered valid, and is incremented by the counter Ngen which records the number of fibers generated. The process is repeated until Ngen≥NFI.

### Application of Boundary Conditions and Loads

The boundary conditions and loads were applied to simulate the four-point bending test as shown in Fig. 4. Constraints were defined at the supports located 5 cm from the beam ends, restricting the displacements in all directions (UX=UY=UZ=0) to simulate the typical fixed conditions of an experimental test [12].

Fig. 4. 4-point bending test configuration adapted from [13]

Nodes were selected on the top face, and the total point load was distributed and divided by the number of selected nodes. A gravitational acceleration of 9.81 m/s² was included to account for self-weight.

## Importing the Model into ANSYS Workbench

Once the initial model was developed in ANSYS APDL, it was transferred to ANSYS Workbench for structural analysis. This step was based on theoretical principles that ensure the consistency of the computational model, to preserve both the geometry of the steel fiber reinforced concrete (SFRC) beam and the associated physical conditions. The transfer respected the laws of solid mechanics, ensuring the correct interaction between the heterogeneous materials.

## Structural Analysis Configuration in ANSYS Mechanical

The structural analysis setup was based on the principles of solid mechanics and cyclic fatigue theory, using the model imported from ANSYS APDL. This process evaluated the mechanical behavior of the SFRC under bending, respecting the interaction between heterogeneous materials. The property assignment was based on theoretical models of elasticity and fatigue strength, integrating S-N curves describing the degradation under repetitive loading, aligning with the accumulated damage theory [12].

### Material Properties and S-N Curves

The fatigue properties of the materials used in the model were defined from the literature review and the data integrated in ANSYS Workbench. For the fiber steel, the S-N curves preset in the software were used, which reflect the relationship between the alternating stress and the number of cycles to failure, following a typical logarithmic behavior, documented in the literature [14]. This behavior can be described by Basquin (5), which constitutes a theoretical reference model in the fatigue analysis of metallic materials:

| σa=σf'2Nfb | (5). |
| --- | --- |

Where σa the alternating stress, σf' is the fatigue strength, Nf represents the cycles to failure and b is the fatigue exponent. This equation provides the conceptual framework that allows relating the applied stresses to the fatigue life of the steel.

In the case of concrete, the relationship between the number of cycles and alternating stress was defined from S-N curves, taking as a reference the work [15], The study examined the fatigue behavior of fiber-reinforced and conventional concrete. These data were selected for their relevance and for covering a representative range of cycles and stress levels used in flexural tests under repetitive loads.

These data were subsequently implemented in the Fatigue Tool of the software to model the fatigue life of the SFRC beam, allowing for the estimation of the progressive degradation of the materials under cyclic loading.

## Fatigue Tool Configuration

The fatigue tool setup was used for estimate the service life of the SFRC beam under repetitive loads. This analysis was supported by the S-N curves defined in the previous section for steel and concrete. The model was constructed using the last static analysis as a basis for simulating behavior under load cycles.

### Cyclic Loading and Stress Correction Parameters

For the Fatigue Strength Factor (Kf), it was set to 1, indicating that no additional adjustment was applied to the fatigue strength of the material. This factor is used to consider effects such as stress concentrations or complex geometries.

The configuration of the loads was established with the Zero-Based type, which implies that there was a relationship of stresses where R=0.

| R=σmin σmax | (6). |
| --- | --- |

Fig. 5 shows the behavior of the stress ratio when the stress ratio equals to zero.

Fig. 5. Graph depicting a stress ratio equal to zero

As for the Mean Stress Theory, Goodman's Theory, (7) [16], was adopted to correct the mean stress level in the loading cycles.

| σaSe+σmSu=1 | (7). |
| --- | --- |

Where:

σa= stress amplitude

σm= mean stress

Su= ultimate stress

Se= equivalent stress for σm=0

Goodman's method treats the positive mean stress correction in such a way that the mean stress always accelerates fatigue failure, while ignoring the negative mean stress. This method gives a conservative result for the mean compressive stress. It is shown in Fig. 6.

Fig. 6 Schematic diagram of Goodman's mean stress correction.

### Fatigue Life and Sensitivity Evaluation

The fatigue life assessment was structured on the cumulative damage theory, estimating the number of cycles to failure by integrating S-N curves and cyclic loading conditions. It was assumed that the interaction between concrete and fibers increases the cyclic strength, reducing the rate of microfracture propagation. In addition, the sensitivity of the model was analyzed, considering variability in fiber distribution and residual stresses as factors affecting service life. This approach highlighted the dependence of SFRC durability on load amplitude and material interface quality, providing a basis for predicting failures under real conditions.

The following is a description of each of the parameters evaluated in the fatigue analysis using the ANSYS Workbench Fatigue Tool. First, the "Life" parameter represents the life available for the given fatigue analysis. During a constant amplitude analysis, if the alternating stress is lower than the lowest alternating stress defined in the S-N curve, the life value corresponding to that point is used; in addition, a limit of 1e06 cycles is imposed.

Second, the "Safety Factor" parameter with respect to fatigue failure at a given design life, with a reported maximum FS of 15. The steps for its calculation at each node include, initially, calculating the alternating and mean stress tensors; subsequently, collapsing these tensors to scalar values using the selected stress component; and, finally, calculating the FS from (8). [17] The of mean stress and Se are queried from the S-N curve for the design life. Consequently, this factor provides a conservative measure of structural safety.

| σaSe+σmSu=1nf | (8). |
| --- | --- |

Finally, the "Fatigue Sensitivity" parameter shows how the fatigue results vary as a function of the load at the critical location of the scoped region. This analysis allows evaluating the robustness of the design to load variations, identifying sensitive points where small changes in the amplitude could significantly reduce the service life.

# RESULTS AND DISCUSSION

## Development of the Computational Model in ANSYS APDL

This section discusses the results of the computational model development. The process is structured in several phases. In this step, the geometrical properties of the beam and the steel fibers were defined, including their size, distribution, and volumetric content. Subsequently, the geometry of the beam and its mesh were generated using finite elements suitable for structural analysis. In the next phase, the random distribution of the steel fibers was implemented using a stochastic algorithm. Then, the boundary conditions were applied.

### Definition of Geometric Properties

During this stage, the geometric properties of the computational model were defined and parameterized within the ANSYS APDL environment. The steel fiber reinforced concrete (SFRC) beam was configured as a rectangular prism with a base and height of 15 cm, and a total length of 70 cm, allowing for a free span of 60 cm between supports. These dimensions were transformed to meters in the code preprocessing, ensuring compatibility with the units of the international system.

Steel fibers were defined with a diameter of 0.55 mm and a length of 35 mm, using a volumetric content of 1%. This value was used to automatically calculate the total number of fibers needed to achieve the specified ratio, resulting in 18,941 fibers generated. These were randomly distributed in the beam volume following a stochastic algorithm, the implementation of which is described in a later section.

The parameters calculated during this phase of the computational model, derived directly from the input values and automated processing in ANSYS APDL, are summarized in the Table. 3, which includes only the results obtained after geometric definition and initial configuration of the model.

Table. 3. Parameters calculated during the geometrical definition of the SFRC model

| Parameter | Symbol | Value |
| --- | --- | --- |
| Free span between supports(m) | – | 0.6 |
| Number of fibers generated | NFI | 18941 |
| Beam volume(m³) | VOLBL | 0.01575 |
| Volume of one fiber(m³) | VOLFI | 8.32E-08 |
| Modulus of elasticity (Pa) | EC | 2.29E+10 |

### Geometry and Mesh Generation

Once the geometric and material properties of the model were defined, the geometry of the beam and its corresponding meshing were generated in ANSYS Mechanical APDL. The beam was modeled as a rectangular prismatic volume, using the BLC4 command, which allows defining three-dimensional bodies by means of coordinates and dimensions. The initial geometry generated is shown in Fig. 7 a).

For the discretization of the domain, the SOLID186 finite element was used, which corresponds to a 20-node 3D element capable of representing structural solids. This type of element was selected for its robustness for structural analysis.

The mesh size was controlled by the NDIV parameter, which defined integer divisions on the basis of the beam. An iterative refinement of the mesh was implemented, automatically increasing NDIV until ensuring that the number of available nodes was sufficient for the subsequent assignment of steel fibers. This process culminated with a final value of NDIV = 11, after 4 iterations of refinement (ITER value), reaching a total of 53,254 nodes (NUMAX) and 36,160 elements (NELEM1) in the structural mesh, as shown in Fig. 7 b).

a)

b)

Fig. 7. Model geometry and meshing

This procedure ensured that the beam geometry and spatial discretization met the requirements for subsequent fiber insertion, structural analysis and fatigue study.

### Random Distribution of Steel Fibers

The distribution of the steel fibers within the concrete beam model was implemented randomly using a stochastic algorithm in ANSYS APDL. This approach allows the assignment of fibers with a non-uniform distribution and the insertion of the fibers within the beam volume, following methods similar to those used by Bolander and Saito [18] in their modeling of short fibers in cementitious composites.

The final model included a total of 18,941 fibers, with a homogeneous distribution in space, as shown in Fig. 8.

Fig. 8. Random distribution of steel fibers within the beam volume Representation of the three-dimensional distribution of fibers within the beam, using the LINK180 element.

The fiber assignment process consisted of randomly selecting a node within the beam volume, determining its direction in three spatial axes by random rotations, and spreading the fibers along these nodes.

### Application of Boundary Conditions

Once the geometry and meshing of the model were defined, the boundary conditions and corresponding loads were applied to simulate the structural behavior. The beam was modeled as a supported structure, with restraints at both ends to simulate the supports.

Bending loads were applied to the beam at specific points, simulating a load distributed over the beam area. A load was defined and distributed among the selected nodes, in accordance with the loading conditions specified in the methodology. Fig. 9 shows how the boundary conditions and applied loads are represented in the model, with the supports at the ends and the loads distributed across the width of the beam.

Fig. 9. Application of boundary conditions

## Importing the Model into ANSYS Workbench

Once the geometric definition, mesh, and boundary conditions were completed in ANSYS APDL, the next step was to import the model into ANSYS Workbench to perform the structural and fatigue analysis of the steel fiber reinforced concrete (SFRC) beam. The import of the model from the APDL environment to Workbench was performed through a database file (.cdb), which contains all the structural, geometric, and material information of the model.

The import process started with the generation of the .cdb file in ANSYS APDL, using the CDWRITE command, to export all relevant model information, including geometry, meshing, material properties, and boundary conditions. Subsequently, the .cdb file was loaded into ANSYS Workbench using the ANSYS Mechanical component, which allows the model to be viewed and edited for more advanced analysis. In Workbench, the imported material properties, mesh, and boundary conditions were verified, ensuring that the data transfer was performed correctly. Finally, once the model was imported, the results of the import were reviewed, including the correct assignment of material properties and boundary conditions, and the meshing was verified to be adequate for the intended analyses, making adjustments if necessary.

## Structural Analysis Configuration in ANSYS Mechanical

This section describes the procedure followed to set up the structural analysis in ANSYS Mechanical Workbench, starting from the geometrical, material, and fatigue data previously defined in APDL. The process included the assignment of mechanical properties to materials, the incorporation of S-N curves as input data for fatigue life analysis.

## Material Properties and S-N Curves

For the fiber steel, the S-N curves included in ANSYS Workbench were used, which represent the characteristic behavior of this material under cyclic loading. These curves show how the alternating stress decreases as the number of cycles increases, following a typical logarithmic trend described in Basquin's equation and documented in the literature [14]. The values used in the simulation are summarized in the Table. 4.

Table. 4. Steel S-N curve data

| Cycles | Alternating Stress (Pa) |
| --- | --- |
| 10 | 4.00E+09 |
| 20 | 2.83E+09 |
| 50 | 1.90E+09 |
| 100 | 1.41E+09 |
| 200 | 1.07E+09 |
| 2000 | 4.41E+08 |
| 10000 | 2.62E+08 |
| 20000 | 2.14E+08 |
| 100000 | 1.38E+08 |
| 200000 | 1.14E+08 |
| 1000000 | 8.62E+07 |

Fig. 10 illustrates the S-N curve of steel, which exhibits a significant decrease in stress during the first cycles and subsequent stabilization in the high fatigue cycle region, typical behavior of metallic materials such as steel.

Fig. 10. S-N curve of steel

In the case of concrete, the input data for the S-N curve were obtained from [15], who experimentally documented the fatigue behavior of plain and Fiber-Reinforced concrete. These data were selected for their relevance in the simulation, covering a representative range of load cycles and alternating stresses. The values used are presented in the Table. 5.

Table. 5. Simple concrete S-N curve data

| Cycles | Alternating Stress (MPa) |
| --- | --- |
| 10 | 25.26 |
| 20 | 24.81 |
| 50 | 24.22 |
| 100 | 23.77 |
| 200 | 23.32 |
| 2000 | 21.83 |
| 10000 | 20.79 |
| 20000 | 20.34 |
| 100000 | 19.30 |
| 200000 | 18.85 |
| 1000000 | 17.81 |

The graphical representation of the S-N curve of concrete (Fig. 11) shows how the alternating stress decreases progressively with the increase in the number of cycles, following a logarithmic trend with some dispersion of the experimental points. The obtained fit presented a coefficient of determination of R²=0.6606, which indicates the influence of other factors on the fatigue behavior of this material [15].

Fig. 11. S-N curve for plain concrete, adapted from [15]

Together, the S-N curves of steel and concrete allowed us to establish the necessary input parameters for the fatigue life analysis of the Fiber-Reinforced beam. While the steel showed a more predictable and stable behavior in the high-cycle region, the concrete presented a larger scatter in the experimental data, reflecting its heterogeneous nature. These results form the basis on which the simulations were developed in ANSYS Workbench.

## Static analysis

The static analysis evaluated SFRC beams under four-point bending. The maximum deflections were 0.34831 mm (0%), 0.34784 mm (0.14% less at 1.0%) and 0.2834 mm (22.74% less at 1.5%). The maximum Von Mises stresses decreased from 48.757 MPa (0%) to 48.728 MPa (0.06% less at 1.0%) and 44.382 MPa (9.79% less at 1.5%).

The stress distribution became more uniform with fibers, reducing peaks by 5-10% in critical zones. Results in Table 6 confirm improvement with 1.5% Vf.

Table 6. Static analysis results.

| Case | % Fibers | Max. deflection (mm) | % Reduction Def. | From Mises Máx. (MPa) | % Effort Reduction |
| --- | --- | --- | --- | --- | --- |
| 1 | 0% | 0.34831 | - | 48.757 | - |
| 2 | 1.00% | 0.34784 | 0.14% | 48.728 | 0.06% |
| 3 | 1.50% | 0.2834 | 22.74% | 44.382 | 9.79% |

Fig. 12 illustrate deformation and Von Mises stress distributions. This supports the enhanced load-bearing capacity of SFRC under elevated static loads.

Fig. 12 Deformation and Von Mises Stress Distributions

Fig. 12 presents the distribution of Von Mises stresses and total deformations for the case with 1.5% fibers. The maximum stress of 44.382 MPa is concentrated at the intrados, while the maximum deformation of 0.2834 mm occurs at the lower center. This figure demonstrates the reduction and uniformity achieved with the highest fiber content.

## Fatigue Analysis

Fig. 13 shows the results obtained from the fatigue analysis for three percentages of steel fibers (0.0%, 1.0% and 1.5%). The color maps show, in the first row, the safety factor distribution, while the second row shows the fatigue life distribution (in number of cycles). This arrangement allows a visual comparison of how the addition of fibers modifies both the strength and durability of the material under cyclic loading.

Fig. 13 Comparison of safety factor and fatigue life as a function of steel fiber percentage.

The results show that, although the safety factor remained close for the three cases, the reinforcement with steel fibers (1.0% and 1.5%) generated a slight increase in the critical zones with respect to concrete without fibers. Regarding the fatigue life, it can be seen that the reinforcement delayed the appearance of failures, extending the duration in cycles before collapse.

A quantitative comparison is made with the results of [19]. They used the extended finite element method (XFEM) at 3D mesoscale. Their setup involved cyclic loads at 70 kN and 5 Hz. It was validated with experimental beam tests, showing only a 4.2% deviation in fatigue life prediction.

Its analysis covered fiber volume fractions (Vf) from 0.5% to 2.5%. Fatigue lives of between 1.70x106 and 2.0106cycles were obtained for optimal fiber aspect ratios (e.g., 30/0.55 and 30/0.35 mm length/diameter). This agrees with our ANSYS Workbench results, where models with one load showed lifetimes around 106 cycles.

Notably, [19] found improvements in fatigue life with higher Vf. This included a 51% increase from 0.5% to 1.0% Vf and a 28% increase from 1.0% to 1.5% Vf. These trends mirror our factor of safety (FS) values, increasing from 0.506 (0% fibers) to 0.531 (1.0% fibers, 4.9% relative improvement) to 0.566 (1.5% fibers, further 6.6% relative improvement).

Table 7 shows the safety factor values obtained in each of the cases analyzed. It is important to note that these values do not imply that the beam will fail with a load lower than the applied load; in this case, it was used as a comparative parameter to evaluate the evolution of the structural behavior against fatigue by increasing the reinforcement with steel fibers.

Table 7. Safety factor values as a function of the percentage of steel fibers.

| Case | Pf | safety factor |
| --- | --- | --- |
| 1 | 0.0% | 50.55% |
| 2 | 1.0% | 50.63% |
| 3 | 1.5% | 56.60% |

Fig. 14 shows the fatigue sensitivity obtained for the cases analyzed with steel fiber percentages of 0.0%, 1.0% and 1.5%. In all cases, it is observed that the fatigue life is maintained in the order of 10e6 cycles until reaching a critical threshold in the loading history, from which an abrupt decrease in the life capacity occurs. The reinforcement with steel fibers slightly delays the onset of this drop, showing that the percentages of 1.0% and 1.5% present a better performance compared to unreinforced concrete. However, the trend of sudden collapse of fatigue life was maintained in all cases, indicating a characteristic brittle behavior in the final stage of repetitive loading.

Fig. 14 Fatigue sensitivity for different percentages of steel fibers (PF)

The vertical axis shows the available fatigue life (number of cycles) in a logarithmic scale, while the horizontal axis shows the normalized load history, which indicates the evolution of the stress applied during the cyclic process.

# Conclusions

The present study demonstrated that computational modeling is a robust tool to analyze the fatigue behavior of steel fiber reinforced concrete (SFRC) beams. The results showed that the incorporation of fibers positively modifies both the stress distribution and the durability of the material, delaying the occurrence of failure under repetitive loading. Thus, the effectiveness of the numerical approach to reproduce trends observed in experimental studies reported in the literature was proven.

Regarding the comparative analysis, it was observed that the increase in the percentage of steel fibers generated slight improvements in the safety factor and a longer fatigue life before collapse. Although the safety factor values remained close in all cases, the reinforcement allowed extending the duration of the cycles and improving the performance compared to concrete without fibers. Fatigue sensitivity, however, is a brittle behavior in the final stage, with abrupt drops in life, suggesting that the material maintains vulnerabilities inherent to its heterogeneous nature.

The findings of this study can be utilized in the design and enhancement of SFRC beams and other structural components exposed to cyclic loading, thereby fostering safer and more resilient infrastructure.

Finally, it is recommended, for further studies, to explore different fiber proportions and morphologies, as well as more complex loading conditions that include variability in amplitudes and sequences. Also, experimental validation of the numerical models presented here would strengthen their practical applicability and open the door to more accurate design recommendations for SFRC structures subjected to cyclic loading.

Disclaimer (Artificial intelligence)

Author(s) hereby declare that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc.) and text-to-image generators have been used during the writing or editing of this manuscript.

# REFERENCES

[1]	C. Frazão, J. Barros, J. A. Bogas, V. García-Cortés, and T. Valente, “Technical and environmental potentialities of recycled steel fiber reinforced concrete for structural applications,” Journal of Building Engineering, vol. 45, 2022, doi: 10.1016/j.jobe.2021.103579.

[2]	V. S. Kuntal, P. Jiradilok, J. E. Bolander, and K. Nagai, “Estimating corrosion levels along confined steel bars in concrete using surface crack measurements and mesoscale simulations guided by model predictive control,” Cem Concr Compos, vol. 124, 2021, doi: 10.1016/j.cemconcomp.2021.104233.

[3]	C. Xie, M. Cao, M. Khan, H. Yin, and J. Guan, “Review on different testing methods and factors affecting fracture properties of fiber reinforced cementitious composites,” Constr Build Mater, vol. 273, 2021, doi: 10.1016/j.conbuildmat.2020.121766.

[4]	A. Tarawneh, G. Almasabha, R. Alawadi, and M. Tarawneh, “Innovative and reliable model for shear strength of steel fibers reinforced concrete beams,” Structures, vol. 32, pp. 1015–1025, 2021, doi: 10.1016/j.istruc.2021.03.081.

[5]	L. Li, M. Khan, C. Bai, and K. Shi, “Uniaxial tensile behavior, flexural properties, empirical calculation and microstructure of multi-scale fiber reinforced cement-based material at elevated temperature,” Materials, vol. 14, no. 8, 2021, doi: 10.3390/ma14081827.

[6]	M. Fakoor and M. Nematzadeh, “Evaluation of post-fire pull-out behavior of steel rebars in high-strength concrete containing waste PET and steel fibers: Experimental and theoretical study,” Constr Build Mater, vol. 299, 2021, doi: 10.1016/j.conbuildmat.2021.123917.

[7]	H. Dehghanpour, S. Subasi, S. Guntepe, M. Emiroglu, and M. Marasli, “Investigation of fracture mechanics, physical and dynamic properties of UHPCs containing PVA, glass and steel fibers,” Constr Build Mater, vol. 328, 2022, doi: 10.1016/j.conbuildmat.2022.127079.

[8]	X. Le, “Fundamentals of Finite Element Analysis (FEA),” 2025, pp. 47–77. doi: 10.1007/978-3-031-64132-9_2.

[9]	M. Mishra et al., “A bibliometric analysis of sustainable development goals (SDGs): a review of progress, challenges, and opportunities,” Environ Dev Sustain, vol. 26, no. 5, pp. 11101–11143, May 2024, doi: 10.1007/S10668-023-03225-W/METRICS.

[10]	“Basic Analysis Guide,” 2023. [Online]. Available: http://www.ansys.com

[11]	M. R. Carvalho, J. A. O. Barros, Y. Zhang, and D. Dias-da-Costa, “A computational model for simulation of steel fibre reinforced concrete with explicit fibres and cracks,” Comput Methods Appl Mech Eng, vol. 363, p. 112879, May 2020, doi: 10.1016/j.cma.2020.112879.

[12]	B. Boulekbache, M. Hamrat, M. Chemrouk, and S. Amziane, “Flexural behaviour of steel fibre-reinforced concrete under cyclic loading,” Constr Build Mater, vol. 126, pp. 253–262, 2016, doi: 10.1016/j.conbuildmat.2016.09.035.

[13]	“Test Method for Flexural Strength of Concrete (Using Simple Beam with Third-Point Loading),” Mar. 01, 2022, ASTM International, West Conshohocken, PA. doi: 10.1520/C0078_C0078M-22.

[14]	J. Schijve, “Fatigue of structures and materials,” Fatigue of Structures and Materials, pp. 1–622, 2009, doi: 10.1007/978-1-4020-6808-9/COVER.

[15]	M. K. Lee and B. I. G. Barr, “An overview of the fatigue behaviour of plain and fibre reinforced concrete,” Cem Concr Compos, vol. 26, no. 4, pp. 299–305, May 2004, doi: 10.1016/S0958-9465(02)00139-7.

[16]	J. Schijve, Fatigue of Structures and Materials. 2008. doi: 10.1007/978-1-4020-6808-9.

[17]	A. Tzanetos and M. Blondin, “A qualitative systematic review of metaheuristics applied to tension/compression spring design problem: Current situation, recommendations, and research direction,” Eng Appl Artif Intell, vol. 118, p. 105521, Feb. 2023, doi: 10.1016/J.ENGAPPAI.2022.105521.

[18]	J. E. Bolander and S. Saito, “Discrete modeling of short-fiber reinforcement in cementitious composites,” Advanced Cement Based Materials, vol. 6, no. 3–4, pp. 76–86, Oct. 1997, doi: 10.1016/S1065-7355(97)90014-6.

[19]	F. Yang et al., “Numerical analysis of fatigue performance of steel fiber reinforced concrete pavement based on microscopic crack growth theory,” Advances in Bridge Engineering, vol. 6, no. 1, p. 33, Oct. 2025, doi: 10.1186/s43251-025-00180-6.