Deployment of Artificial Intelligence for Optimising Scaffolds Design and Production in Tissue Engineering: A Critical Overview

# Abstract

The synergy of Artificial Intelligence (AI) technology and Tissue Engineering (TE) is creating a new frontier in regenerative medicine. Conventional design of scaffolds for enhancing cell attachment, growth and differentiation is well reported to be achieved through experimental methods. The AI is an emerging technique offering a powerful computational approach that can be deployed to analyse nonlinear and other complex interactions between different scaffold parameters. The foregoing makes it possible to predict and improve designs more efficiently. In this work, attempt is made to critically review the use of AI from traditional machine learning models to advanced deep learning systems for improving scaffold structure, composition and biological performance. Critical attention is made to the roles of supervised and unsupervised learning in predictive modelling, the use of generative algorithms for structural design and the application of evolutionary methods for optimising multiple design objectives. The synergy between AI, computational biomechanics, finite element modelling and Additive Manufacturing (AM) is examined, showing how innovations such as digital twin technology and automatic bioprinting have emerged. The review also explores how AI is deployed for material selection, surface property prediction and biodegradability evaluation in composite materials. Current challenges such as limited data, difficulty in model interpretation and ethical considerations are well discussed along with future directions that include physics-informed networks and combined AI systems. This review underscores the progress that has been made in the deployment of AI technology for optimisation of scaffold design, its production and subsequent application for improved accuracy, consistency and personalisation in regenerative medicine.

Keywords:  Scaffold optimisation, AI systems, Machine learning models, Deep learning systems, Regenerative medicine

# 1. Introduction

In the last three decades, Tissue Engineering (TE) has evolved into one of the most progressive areas within regenerative medicine. The hallmark aim is to repair, replace or improve the function of damaged tissues by combining scaffolds, living cells and biological signaling agents (Brown and Badylak, 2022). In this regard, scaffold is quintessential as the structural base that facilitates cell attachment, multiplication, and specialisation, while maintaining its mechanical strength and allowing the movement of nutrients (Zhang et al., 2023). Designing scaffolds that have good biological compatibility characteristics without compromising their mechanical and structural integrity properties continues to present difficulties. This can be attributed to the interactions between material structure, physical properties and cellular responses that are generally complex and nonlinear. Traditionally, optimising scaffold performance has been guided by experimental trial and error, which consumes time and resources and often lacks consistency. The growing use of artificial intelligence now provides a data-based method that can predict scaffold behavior and improve its design with high precision (Li et al., 2024).

Artificial Intelligence (AI) refers to the ability of computer systems to imitate human reasoning and learning, has shown outstanding potential across many medical applications, including drug discovery, imaging, and personalised diagnostics (Jiang et al., 2023). In TE, it provides analytical tools capable of processing large volumes of experimental, imaging, and simulation data. These computational models can reveal hidden connections between scaffold design parameters including porosity, surface texture, rate of degradation and mechanical performance. Uncovering these patterns provides a platform for researchers to move from guesswork towards a reliable rational scaffold design (Wu and Chen, 2023). Machine learning and deep learning approaches are able to predict how cells interact with scaffolds and how materials degrade in biological environments. Such predictive strength improves the selection of materials, speeds up fabrication, shortens design cycles and increases experimental reproducibility, which is crucial for clinical success.

The application of AI in scaffold development has become possible through advances in rapid data collection and computational simulation. Techniques including micro Computed Tomography(CT) confocal microscopy and atomic force imaging for producing detailed datasets that describes scaffold microstructure and surface chemistry. At the same time, finite element modeling generates artificial datasets that simulate mechanical stress and transport behaviour within scaffolds (Shen et al., 2022). The AI algorithms can merge these different datasets to learn how design factors influence biological outcomes and enabling balanced optimisation of multiple goals. For instance, genetic algorithms and particle swarm optimisation have been used to find the best combination of porosity, rigidity, and degradation rate (Kumar and Singh, 2023). Through the interaction between modelling and experimentation, scaffold design can be refined in a continuous feedback loop.

Nevertheless, the use of AI for scaffold optimisation is still limited by several challenges. A lack of extensive datasets remains a serious issue because most experimental studies in TE includes small sample numbers and inconsistent reporting methods (Ahmed et al., 2021). Moreover, many AI models act as opaque systems that provide accurate predictions, but little explanation of the chemical or physical principles behind them. Overcoming this limitation may require mixed modelling strategies that combine data learning with theoretical understanding, as seen in physics informed neural networks (Ma and Zhao, 2024). Ethical matters related to data ownership, bias in algorithms, and openness in Intellectual Property (IP) also affect the acceptance of these technologies in clinical fields. Addressing these problems will require strong collaboration among engineers, material scientists, computer specialists and healthcare professionals.

This review provides a detailed assessment of how AI is being integrated into scaffold design for TE. It explains the main groups of AI techniques such as supervised and unsupervised learning, deep learning, and evolutionary computation, highlighting their roles in improving scaffold construction and performance evaluation. The review also explores how AI connects with AM and digital twin systems for predictive fabrication. Finally, it points out current barriers in data consistency, model transparency, and regulatory approval, while discussing future possibilities for developing adaptive and patient specific scaffolds. The union of AI and TE signals a shift from traditional experimental methods to intelligent, automated, and predictive design of biomaterials.

# 2. Conceptual Framework

The incorporation of AI into scaffold development for TE is built on a broad interdisciplinary foundation that connects biomaterial research, computational modelling, and data analysis. This combined framework offers a structured method for exploring how AI tools can simulate, forecast, and improve the link between scaffold structure and performance in regenerative medicine. Essentially, it converts the complex interactions between biological systems and material properties into models that computers can analyse, allowing for intelligent and automated decisions in scaffold design and evaluation (Wang et al., 2023).

# 2.1 Scaffold Design Principles in TE

A scaffold functions as a three dimensional matrix that imitates the natural extracellular matrix, providing both physical and chemical signals that support cell attachment, multiplication, and specialization (Liu et al., 2022). The effectiveness of a scaffold depends on a combination of architectural, physical, and biological properties such as pore diameter, overall porosity, surface texture, level of water attraction, stiffness, rate of degradation, and the inclusion of bioactive compounds (Zhang et al., 2023). In most cases, traditional scaffold design has been guided by experimental adjustments in which researchers manually alter these parameters to obtain the desired cellular reaction, as illustrated in Figure 1. However, this method often demands significant time and produces variable results because of the inherent differences in biological samples and the limited repeatability of manual approaches.

Figure 1: Schematic of Theory behind TE (Roberts et al., 2008)

To overcome these challenges, the conceptual model identifies AI as a  computational link that can learn and interpret complex relationships between design variables and biological outcomes. By combining information obtained from mechanical characterisation, cellular experiments and various imaging techniques, artificial intelligence systems can reveal hidden trends that are difficult to express through direct mathematical modeling. For example, supervised learning methods are capable of predicting how well cells adhere or remain viable based on the microscopic structure and surface properties of scaffolds. In contrast, unsupervised learning techniques can organize or group scaffold samples according to similarities in their internal architecture (Kim et al., 2021). The knowledge derived from these analyses supports logical scaffold design and allows continuous improvement through iterative feedback and model refinement.

# 2.2 The AI Paradigms Relevant to Scaffold Optimisation

According to Huang et al. (2022), AI includes a wide range of computational approaches, among which machine learning, deep learning, and evolutionary algorithms are the most prominent. Each of these approaches contributes uniquely to the improvement of scaffold design in TE. Machine learning focuses on creating predictive systems that are trained on well-labeled datasets to uncover relationships between scaffold design variables, such as porosity or stiffness, and performance indicators like mechanical strength or the rate of cell growth. Although models such as regression analysis, support vector machines and random forests have proven effective in interpreting complex datasets with many variables, their prediction accuracy often decreases when applied to highly irregular or limited biological data.

Deep learning represents a more advanced branch of machine learning that employs networks made up of several processing layers to learn complex data patterns. Xu et al. (2023) reported that convolutional neural networks (CNNs), a type of deep learning model, have achieved impressive performance in interpreting scaffold images obtained from scanning electron microscopy and micro CT. Sequel to the foregoing, deep learning methods can detect structural features that influence how cells attach to materials and how tissues develop within them. Nevertheless, these models generally require large volumes of labelled data and strong computing power, which are often unavailable in many biomaterials research environments. As a result, their widespread use in scaffold engineering is still limited, particularly in laboratories with restricted access to computational infrastructure.

In addition, evolutionary algorithms such as genetic algorithms, particle swarm optimisation, and ant colony optimisation apply random search principles inspired by natural evolution to solve optimisation challenges involving multiple competing goals (Singh and Ramesh, 2023). These techniques are especially valuable in adjusting scaffold materials and geometry when it is necessary to balance factors such as porosity and mechanical durability. Despite their effectiveness, evolutionary algorithms demand heavy computation and can require many iterations before achieving a stable result. However, when properly tuned, they demonstrate a high level of flexibility in exploring complex design conditions. Combining evolutionary algorithms with machine learning or deep learning frameworks can therefore strengthen model robustness and improve the accuracy of scaffold performance predictions.

# 2.3 Data-Driven Scaffold Optimisation Workflow

The conceptual model brings together data collection, algorithm training, and predictive analysis within a single continuous workflow, as illustrated in Figure 2. The procedure starts with the creation of reliable datasets obtained from experimental and analytical methods such as scanning electron microscopy, Fourier transform infrared spectroscopy, X ray diffraction, and mechanical evaluation. These collected data contain quantitative details that describe the structural, chemical, and mechanical properties of the scaffold materials. Before being used for model development, the raw data are processed to remove inconsistencies, standardised for uniform scaling and then divided into suitable subsets for training and validation of the artificial intelligence models.

Figure 2: Conceptual Framework for AI-Based Scaffold Optimisation

Hosseini et al. (2022) reported that well-trained AI systems can estimate important indicators of scaffold performance such as compatibility with living tissues, rate of degradation and elastic modulus. These predictions are verified through laboratory experiments and the resulting data are fed back into the computational model for further retraining, forming a continuous learning and improvement cycle. This feedback-driven process enhances the adaptability of the model and supports the development of scaffolds that progressively approach optimal biological performance. Nevertheless, although this method improves prediction reliability, its success still relies heavily on the accuracy and consistency of experimental data. When biological variability is considerable, repeated feedback can unintentionally maintain or magnify systematic errors rather than remove them.

In more advanced research, AI has been increasingly combined with AM and computational fluid dynamics simulations to achieve greater precision and biological realism in scaffold design (Mohan et al., 2024). Within this combined framework, AI algorithms can automatically adjust three dimensional printing conditions such as feed rate, layer thickness, and printing temperature to preserve structural detail and ensure reproducibility of the printed scaffolds. At the same time, computational fluid dynamics models help analyse how nutrients and oxygen move through scaffold pores, allowing the algorithm to refine transport properties and improve the survival of developing tissues. However, merging these techniques introduces technical complexity, especially when coordinating data exchange across multiple real time systems. When this synchronisation is well established, the combination allows intelligent automation, process correction during fabrication, and predictive control. This integration therefore represents a major advancement toward responsive and data oriented design strategies in regenerative medicine.

# 2.4 Theoretical Integration of AI with TE

From a theoretical standpoint, the connection between AI and TE follows the principles of systems biology and computational biomaterials science, both of which seek to describe biological behavior through mathematical and data-based models. This relationship makes it possible to convert molecular and cellular activities into measurable variables that can be adjusted computationally (Almalki and Alghamdi, 2023). In scaffold development, artificial intelligence supports modeling at multiple scales, linking atomic and nanoscale composition with larger scale mechanical and structural performance. This bridge between biological observations and engineering design enhances understanding and precision in scaffold creation.

The conceptual structure emphasises that AI does not replace biological knowledge or laboratory testing. Instead, it extends them by improving predictive ability and design efficiency. Through this union, scaffold development evolves from a primarily experimental process into one guided by data and knowledge, where model predictions inform hypotheses and testing. This progression represents a decisive move toward personalised tissue engineering, allowing scaffold properties to be tailored to the individual patient’s anatomy and physiological needs.

# 3. Role of AI in Scaffold Design and Optimisation

Integrating AI into scaffold engineering marks a fundamental transition from empirical experimentation to data-driven precision. By using machine learning, deep learning, and hybrid computational methods, researchers can simulate and forecast scaffold performance, leading to materials with customized physical, chemical, and biological characteristics (Li et al., 2024). The capability of AI to interpret complex, high-dimensional data enables predictive modeling of interactions between cells and scaffolds, mechanical response, and degradation behaviour—key parameters that determine successful tissue repair. This section examines how AI techniques contribute to the design, optimisation, production and evaluation of scaffolds, emphasising their impact on data-based biomaterials research.

## 3.1 The AI in Scaffold Design

The aim of scaffold design in tissue engineering is to achieve a balance between biological compatibility, structural stability, and controlled degradation, while reproducing the properties of the natural extracellular matrix (Zhang et al., 2023). Conventional design strategies depend on repeated experimental adjustments to identify suitable pore size, connectivity, and material ratios. Such methods are slow and often uncertain. Artificial intelligence introduces analytical tools capable of identifying complex, nonlinear relationships between variables, thus accelerating the optimization process (Mohan et al., 2024).

## 3.1.1 Machine Learning for Design Prediction

Machine learning algorithms such as support vector machines, random forests and gradient boosting repressor have been employed to estimate scaffold behaviour based on chosen design variables. Liu et al. (2022) demonstrated that these models can accurately predict the tensile and compressive strengths of polymer scaffolds using porosity and layer thickness as inputs. Such predictive models minimise experimental workload by suggesting the best design combinations before fabrication. Moreover, Bayesian optimisation, a probabilistic approach within machine learning, has been applied to identify geometric structures that achieve several objectives at once—for example, maximizing porosity while maintaining structural stability (Kumar and Singh, 2023). This approach is especially valuable for scaffolds meant to support mechanically active tissues such as bone or cartilage.

### 3.1.1.1 Bayesian Optimization for Multi-Objective Scaffold Design

Bayesian optimisation has emerged as a powerful probabilistic framework for resolving difficult design problems in scaffold research, particularly when direct experimentation is expensive or time consuming. It makes use of a surrogate model most often Gaussian process regression to estimate unknown functions and gradually guide the search toward the most favorable solution (Shahriari et al., 2016; Kumar and Singh, 2023). In the field of bioprinted scaffold optimisation, Bayesian optimisation allows the simultaneous adjustment of several structural variables such as pore diameter, strut width, and lattice orientation, producing a well balanced design that maintains both porosity and mechanical strength. The optimisation challenge can be represented mathematically as a problem involving multi-objective problem (Kumar and Singh, 2023; Liu et al., 2022).

Maximize f1​x= Porosityx                                                                               1

and minimize f2​x=Elastic Modulus Deviationx                                          2

subject to design variables x=[pore size, strut thickness, lattice angle]    3

Since porosity and mechanical strength typically exhibit an inverse relationship, the objective of the Bayesian model is to determine scaffold geometries that increase porosity, while maintaining sufficient load-bearing capacity, a key requirement for bone and cartilage regeneration (Zhang et al., 2021).

### 3.1.1.2 Bayesian Model and Surrogate Estimation

In Bayesian optimisation, the unknown function f​x  is modeled as a Gaussian process (GP) to capture both the mean response and associated uncertainty (Rasmussen and Williams, 2006):

fx= ∼GPmx,κx,x'                                                                                     4

where mx is the mean function and κx,x' is the covariance (kernel) function that quantifies similarity between data points.

Given initial data samples xi, fxi , the posterior mean and variance for new inputs x*​​ ​ are updated as follows(Rasmussen and Williams, 2006; Mockus, 2012):

μx*​​= κ​*T(K+σ2I)-1y                                                                                   5

σ2xn= k x*, x*- κ​*TK+ σ2I)-1κ​*                                                                6

Equations (5) – (6) represent the Bayesian updating step, where predictions and uncertainties are continuously refined as new data points are added, forming the foundation of the surrogate model.

### 3.1.1.3 Acquisition Function and Iterative Improvement

The next evaluation point in Bayesian optimisation is selected by maximising an acquisition function, which represents a mathematical measure of potential improvement or utility. Among the various options, the expected improvement (EI) function is the most frequently adopted (Jones et al., 1998).

### 3.1.1.4 Multi-Objective Bayesian Optimisation (MOBO)

When scaffold design involves several competing goals, Multiobjective Bayesian Optimisation extends the Gaussian Process Regression framework to estimate each objective function  f1, f2,…,fn,  individually. This approach constructs a Pareto boundary to highlight nondominated design options that balance mechanical stability with biological performance (Hernández-Lobato et al., 2016). Through this method, researchers can quickly approximate the region where porosity and mechanical strength reach an acceptable equilibrium. For example, Kumar and Singh (2023) found that Bayesian optimisation successfully identified scaffold models achieving more than 80 percent porosity, while preserving compressive strength within the ideal range for bone tissue applications. ​

## 3.1.2 Generative Design Using AI

The AI has made generative design a practical approach in scaffold engineering. By merging computational creativity with data-informed learning. The AI systems can automatically generate structural designs that meet specified functional targets (Chen et al., 2023). Frameworks such as Generative Adversarial Networks and Variational Autoencoders can produce new scaffold geometries that resemble natural extracellular matrix structures while optimising their mechanical attributes. These models rely on large datasets from microcomputed tomography and electron microscopy to learn realistic structural details.

A study by Shen et al. (2022) demonstrated that generative adversarial models produced lattice structures with multiple pore sizes, improving cell growth and nutrient flow. Such AI-based generative methods represent a shift from descriptive modeling to prescriptive creation, where algorithms suggest innovative configurations beyond conventional intuition.

## 3.2 The AI in Scaffold Fabrication

At the fabrication stage, computationally optimised scaffold designs are physically realised through AM and bioprinting. AI contributes by regulating process variables and ensuring repeatability using automated feedback control.

## 3.2.1 Process Parameter Optimisation

Machine-based algorithms now manage 3D printing conditions such as extrusion rate, layer thickness, temperature, and print velocity to prevent defects and preserve fine architectural features. Deep reinforcement learning allows printing systems to automatically adjust operational parameters using sensor feedback in real time (Hosseini et al., 2022). This adaptive regulation ensures consistent pore patterns and mechanical reliability. In addition, neural models can anticipate material flow behavior and fine-tune the viscoelastic properties of bioinks to achieve the necessary balance between structural integrity and cellular compatibility (Wang et al., 2023).

## 3.2.2 Hybrid Modelling with Computational Simulations

Combining numerical simulation with AI supports simultaneous optimisation of structural and biological behaviour. In this setup, finite element analysis generates synthetic datasets of stress–strain behaviour under physiological loading, while AI learns to correlate geometric variables with performance metrics (Wu and Chen, 2023). This results in predictive models capable of recommending design adjustments before physical production begins. Khan et al. (2022) showed that CNN integrated with finite element data successfully identified mechanical failure points in bone scaffolds. This technique accelerates virtual testing, minimising resource consumption and fabrication time.

# 3.3 The AI in Scaffold Characterisation and Performance Prediction

Traditionally, scaffold assessment depends on physical experiments to evaluate morphology, chemical composition, and strength. AI introduces automation into this process, allowing large-scale and precise evaluation.

## 3.3.1 Image-Based Characterisation

Deep learning models such as CNNs can analyze imaging data from SEM, confocal microscopy, and X-ray tomography to quantify structural metrics like pore interconnectivity and surface roughness (Xu et al., 2023). Automated segmentation algorithms eliminate the subjectivity of manual analysis and extract statistically significant descriptors from thousands of images in minutes.
For instance, Mousavi et al. (2023) applied CNNs to classify scaffold microstructures according to fiber orientation and surface texture, achieving over 95% accuracy compared to human experts. Such automated image analysis enhances reproducibility and supports consistent quality control in scaffold fabrication.

## 3.3.2 Predictive Biocompatibility and Cell Response Modeling

Beyond physical analysis, AI algorithms can estimate how cells will behave; whether they attach, multiply, migrate, or specialize based on scaffold properties (Li et al., 2024). Machine models trained on laboratory assay data can anticipate differentiation trends from material composition and morphology. Zhou et al. (2022) reported that artificial neural networks could predict stem cell growth rates with less than 5 percent error, using surface roughness, wettability, and elasticity as predictors. These tools minimize repetitive testing and enable faster material screening.

# 3.4 AI in Scaffold Degradation and Mechanical Optimization

An effective scaffold should gradually dissolve at a pace matching tissue recovery while maintaining adequate structural support. AI contributes by modeling how scaffolds degrade and perform mechanically under real biological conditions.

## 3.4.1 Modeling Biodegradation

Predictive models trained on long-term data can estimate how quickly materials break down and what by-products form in different environments (Ahmed et al., 2021). Support vector regression, for instance, connects polymer composition, crystal structure, and pH to degradation rates, enabling the design of materials that match specific healing durations.

Recent developments have introduced physics-informed neural networks, which combine physical laws with data-based learning to improve transparency and reliability (Ma & Zhao, 2024). This integration ensures that model predictions are consistent with known material principles, addressing the interpretability issue of traditional neural systems.

## 3.4.2 Mechanical Behavior Optimization

AI models can optimize scaffold mechanical performance by correlating microstructure with stress distribution and failure points. Recurrent Neural Networks (RNNs) and Long Short-Term Memory (LSTM) models have been used to predict dynamic mechanical responses under cyclic loading (Huang et al., 2022). Similarly, Genetic Algorithms (GAs) have evolved scaffold structures with improved compressive strength while maintaining 70–80% porosity, achieving better performance than manually designed scaffolds (Singh & Ramesh, 2023). These approaches provide computational blueprints for personalized, load-bearing scaffolds.

# 3.5 Critical Assessment of AI-Driven Scaffold Optimization

While AI enhances predictive power and design efficiency, its implementation in scaffold optimization is not without challenges. The quality and size of datasets remain a bottleneck, as inconsistent experimental reporting and small sample sizes reduce model generalizability (Almalki & Alghamdi, 2023). Moreover, the lack of standardized data formats across studies complicates meta-analyses and multi-lab integration. Another limitation concerns the interpretability of deep learning models, which, although highly accurate, often fail to explain why specific predictions are made. This opacity hinders scientific validation and regulatory acceptance. To address these concerns, researchers are increasingly adopting explainable AI (XAI) approaches that visualize feature contributions and decision pathways (Wang et al., 2023).

Finally, while AI accelerates design and fabrication, its reliability still depends on experimental feedback. AI models must be continuously refined with new biological and material data to maintain accuracy and prevent overfitting.

Despite these limitations, the synergy between AI and tissue engineering continues to redefine scaffold research. The integration of AI-driven insights with experimental validation enables adaptive, efficient, and reproducible scaffold development, marking a critical step toward personalized regenerative medicine.

# 4. Applications of AI in Scaffold-Based TE

The AI applications in scaffold-centered regenerative research go beyond virtual design into real-world biomedical uses that enhance healing outcomes. These computational systems help design biologically inspired scaffolds for tissues such as bone, cartilage, skin, vascular structures and neural networks by predicting material behaviour, guiding fabrication processes, and analysing biological feedback. This multidisciplinary approach bridges material science, biological understanding, and computational modelling to improve regenerative effectiveness.

Table 1: General Overview of AI Applications in Scaffold-Based TE

| Tissue Type | AI Technique / Model | Scaffold-Based Application / Use Case | Key Outcome / Benefit | Representative Study (Author, Year) |
| --- | --- | --- | --- | --- |
| Bone Tissue | Machine Learning (Random Forest, CNNs) | AI-driven design of bone scaffolds with optimized porosity, mechanical strength, and biocompatibility parameters. | Enhanced mechanical prediction accuracy and biologically relevant scaffold geometry. | Kumar & Singh (2023); Zhang et al. (2024) |
| Cartilage Tissue | ML Regression and Support Vector Machines (SVMs) | Prediction of chondrocyte proliferation and extracellular matrix deposition based on scaffold microstructure. | Improved scaffold parameter selection for cartilage mimicry and load-bearing capability. | Patel et al. (2022); Li et al. (2023) |
| Skin / Soft Tissue | Deep Neural Networks (DNN) and Image Analysis | AI-based selection of biomaterials and surface modification for enhanced skin scaffold integration. | Accelerated design cycles and improved wound-healing outcomes. | Oladimeji et al. (2024); Chen & Wang (2022) |
| Neural / Nerve Tissue | Deep Learning (Generative Models, Autoencoders) | Prediction of neural scaffold topologies promoting axonal growth and neural connectivity. | Enabled complex scaffold geometries to support nerve regeneration. | Park et al. (2023); Fernández-García et al. (2022) |
| Dental / Mandibular Tissue | AI/ML Classification and Predictive Modeling | Optimization of scaffold–stem cell interaction for dentin–pulp regeneration using AI-based analysis. | Improved prediction of bioactivity and reduced design-to-experiment time. | Ahmed et al. (2024); Liu et al. (2022) |
| Vascular / Endothelial Tissue | Multi-Objective Optimization (Bayesian, ANN) | AI-guided bioprinting of vascular scaffolds with optimized permeability and flow patterns. | Balanced scaffold porosity, mechanical stability, and perfusion efficiency. | Wang et al. (2023); Gupta & Lee (2024) |
| Muscle / Myogenic Tissue | Reinforcement Learning and Generative Adversarial Networks (GANs) | Predictive modeling of myoblast differentiation on 3D scaffolds. | Achieved better alignment and uniformity in engineered muscle fibers. | Huang et al. (2024); Kim & Zhao (2023) |
| Ocular / Corneal Tissue | Supervised ML and ANN | Optimization of corneal scaffold transparency and mechanical stiffness for vision restoration. | Improved biomaterial composition for optical clarity and biocompatibility. | Ghosh et al. (2022); Martins et al. (2023) |

# 4.1 The AI in Bone TE

Bone Tissue Engineering (BTE) requires scaffolds that possess high mechanical strength, excellent osteoconductivity, and carefully controlled degradation behaviour to promote effective bone regeneration (Kumar and Singh, 2023). The AI methods have played a vital role in addressing these complex design objectives by enabling data-oriented optimisation and predictive modelling. Through the application of techniques such as Artificial Neural Networks (ANN), Support Vector Machines (SVM), and Genetic Algorithms (GA), researchers can identify the optimal combinations of material composition, porosity, and structural geometry that improve scaffold performance and enhance osteogenic potential.

Table 2: Applications of AI in BTE

| AI Technique / Model | Application Area | Key Outcome / Optimization Target | Reference |
| --- | --- | --- | --- |
| Bayesian Optimisation | Scaffold geometry optimisation | Identifies optimal scaffold designs that balance porosity and mechanical integrity for load-bearing applications | Kumar & Singh (2023); Rasmussen & Williams (2006) |
| Machine Learning Regression Models | Mechanical property prediction | Predicts scaffold strength and stiffness based on material composition and fabrication parameters | Zhang et al. (2022) |
| Deep Neural Networks (DNNs) | Cellular response and biocompatibility modeling | Estimates cell adhesion, proliferation, and differentiation from scaffold surface features | Li et al. (2021) |
| Convolutional Neural Networks (CNNs) | Medical imaging and 3D reconstruction | Detects bone defects and assists in patient-specific scaffold fabrication using 3D imaging data | Zhao et al. (2024) |
| Genetic Algorithms (GA) | Multi-objective scaffold optimization | Evolves scaffold parameters to achieve optimal mechanical and biological performance simultaneously | Wang et al. (2023) |
| Generative AI Models (GANs, VAEs) | Novel scaffold structure generation | Creates bioinspired scaffold architectures with improved anisotropy, porosity, and nutrient diffusion | Patel et al. (2024) |

## 4.1.1 Predictive Mechanical and Biological Modelling

The AI frameworks, including ANN, SVM  and Random Forest Regressors (RFR), have been widely utilised to estimate the mechanical performance of bone scaffolds by using parameters such as porosity, strut thickness, and material composition, as illustrated in Fig. 3 (Liu et al., 2022). Li et al. (2024) demonstrated this concept by training an ANN model with experimental datasets to predict the compressive modulus and yield strength of Hydroxyapatite (HA) polymer composites. The resulting system produced an accuracy exceeding 95 percent, significantly reducing the time required for identifying promising formulations. Likewise, machine learning regression models have been employed to evaluate osteoblast proliferation and viability on three-dimensional printed scaffolds using surface roughness and chemical energy values as input variables (Wu and Chen, 2023). This computational pre-assessment technique supports the selection of highly biocompatible materials before experimental confirmation.

Figure 3: Predictive outcome of Mechanical and Biological Modeling

## 4.1.2 The AI-Guided AM

The integration of AI with AM and Computer Aided Design (CAD) has transformed the fabrication of bone scaffolds. Deep Reinforcement Learning (DRL) algorithms are capable of continuously modifying printing parameters to compensate for variations in extrusion rate or temperature during the manufacturing process (Mohan et al., 2024). In a related investigation, Zhang et al. (2023) implemented CNN alongside in situ imaging to monitor scaffold morphology throughout printing, resulting in more than ninety percent print accuracy and a notable reduction in material loss. AI guided AM ensures reproducible quality and further allows the creation of customized scaffolds that conform precisely to patient specific anatomical structures obtained from CT and Magnetic Resonance Imaging (MRI) scans.

Figure 4: (a) Examples of strut based scaffold architectures include the diamond lattice (upper left), the truncated octahedron lattice (upper right), and the cubic lattice (lower left). These lattice geometries contain cylindrical struts with nonzero Gaussian curvature at the points of interconnection. (b) Examples of sheet based scaffold structures include the Neovius sheet scaffold (upper left), a stochastic network scaffold generated from Gaussian random fields (upper right), a Gyroid sheet scaffold (lower left), and a Gyroid network scaffold (lower right). The Neovius and Gyroid configurations represent structures derived from triply periodic minimal surfaces (TPMS). (c) Model prediction of curvature influenced tissue growth on the 0/90 scaffold configuration utilized in vivo by Paris et al. (2019).

Figure 4 displays a range of three dimensional porous scaffold architectures utilized in bone tissue engineering, emphasizing how both strut based and sheet based geometries influence their mechanical and biological behavior as depicted in Figure 5.

(a) Strut Based Scaffolds: This panel shows examples of frameworks such as the diamond lattice (upper left), truncated octahedron lattice (upper right), and cubic lattice (lower left). These structures feature systematically arranged interconnecting struts that allow control over porosity and mechanical strength. The cylindrical struts possess regions of nonzero Gaussian curvature at the connection points, influencing local stress concentration and cell growth behavior (Zhou et al., 2022). Such structural patterns are beneficial for balancing mechanical endurance with adequate nutrient diffusion throughout the scaffold.

(b) Sheet Based Scaffolds: Illustrated here are the Neovius sheet scaffold (upper left), a stochastic network scaffold generated from Gaussian random field modeling (upper right), the Gyroid sheet scaffold (lower left), and the Gyroid network scaffold (lower right). The Neovius and Gyroid configurations originate from Triply Periodic Minimal Surface (TPMS) geometries, distinguished by their continuous curvature and large surface to volume ratios (Hollister, 2021). These characteristics promote even stress dispersion and improved osteogenic cell attachment due to their biomimetic interconnectivity.

(c) Curvature Guided Tissue Growth Simulations: Panel (c) presents computational simulations illustrating tissue development influenced by surface curvature on a 0°/90° scaffold configuration, comparable to the in vivo model described by Paris et al. (2019). The curvature dependent modeling highlights how geometric design affects the rate of tissue infiltration, mechanical anisotropy, and spatial distribution of osteogenic activity. These findings emphasize curvature as a critical variable for designing scaffolds that effectively guide bone tissue regeneration.

Figure 5: Structural Design Categories and Functional Implications of 3D Scaffolds

Table 3: AI-Driven Critical Review of Figure 3: 3D Porous Scaffolds for BTE

| Aspect | Observation / Strength | Critique / Limitation | AI-Based Enhancement / Recommendation |
| --- | --- | --- | --- |
| Clarity and Structure | The figure categorizes scaffolds into strut-based and sheet-based designs. | Lacks clear differentiation between scaffold functions and biological implications. | Use AI-based image segmentation and pattern recognition to automatically classify scaffold types and highlight key geometric differences for clearer visualization. |
| Scientific Depth | Geometric features such as Gaussian curvature are mentioned. | The relationship between geometry and biological response is not quantified. | Apply machine learning regression models to correlate curvature, pore size, and surface topology with experimental data on cell adhesion and proliferation rates. |
| Mechanical and Fabrication Context | Various scaffold architectures are illustrated. | No mechanical data or fabrication method details are linked to the scaffold designs. | Employ AI-driven finite element analysis (FEA) and Bayesian optimization to predict mechanical strength and identify ideal print parameters for each scaffold type. |
| Computational Analysis | Refers to curvature-driven growth predictions. | The description lacks quantitative simulation outcomes or validation metrics. | Integrate AI-assisted growth modeling (e.g., convolutional neural networks trained on tissue growth data) to simulate and visualize curvature-dependent tissue formation. |
| Figure–Text Integration | Mentions multiple sub-panels with descriptive orientation (top left, etc.). | The orientation-based labeling may confuse readers. | Use AI-supported figure annotation tools to generate labeled overlays and automate caption alignment, improving readability and precision. |
| Comparative Insight | Demonstrates structural diversity of scaffold morphologies. | Fails to compare biological and mechanical performance across scaffold types. | Utilize multi-objective AI optimization algorithms to rank scaffold designs based on porosity, mechanical modulus, and predicted biocompatibility for bone regeneration. |

## 4.1.3 Intelligent Biodegradation Control

The degradation behaviour of bone scaffolds should correspond closely with the rate of new tissue formation. The AI models that incorporate polymer chemistry parameters and environmental variables can forecast degradation patterns under physiological settings (Ahmed et al., 2021). Hybrid frameworks such as Physics Informed Neural Networks (PINNs) integrate data driven learning with mechanistic degradation equations, providing both interpretability and precision in prediction (Ma and Zhao, 2024). This approach enables the design of scaffolds with tunable degradation characteristics that maintain mechanical integrity during various stages of bone regeneration.

Figure 6: AI Approach Towards Bone Tissue Engineering using ANN and FEA

Figure 7: AI Approach Towards Cartilage Tissue Engineering using SVR and CNN

# 4.2 AI in Cartilage TE

Cartilage tissue regeneration remains challenging because of its lack of blood vessels and minimal intrinsic healing ability. As illustrated in Figure 6, AI facilitates the precise regulation of scaffold microarchitecture, mechanical response and biochemical cue distribution, all of which are critical for promoting effective cartilage repair.

## 4.2.1 Design Optimisation for Chondrogenesis

Machine learning techniques are increasingly utilized to fine-tune factors that regulate chondrogenic differentiation. For example, Support Vector Regression (SVR) and Gaussian Process Regression (GPR) models have been developed to link scaffold mechanical stiffness, fiber orientation, and pore configuration with Glycosaminoglycan (GAG) accumulation and collagen type II formation (Almalki and Alghamdi, 2023). Through AI-derived design maps, investigators can identify optimal scaffold compositions and geometries that enhance chondrocyte maturation while reducing the need for extensive experimental trials.

## 4.2.2 AI in Bioink and Hydrogel Optimisation

In bioprinting applications, AI facilitates the identification of hydrogel formulations that exhibit optimal rheological and biological performance. Deep learning algorithms can interpret compositional parameters—including polymer concentration, crosslinking intensity, and incorporation of bioactive molecules—to forecast printability and cell encapsulation efficiency (Wang et al., 2023). For instance, Hosseini et al. (2022) employed a CNN to assess hydrogel microstructures and estimate elasticity from SEM imagery, achieving strong correlation between predicted and experimental outcomes. This AI-guided strategy enables consistent and reliable fabrication of cell-laden scaffolds for cartilage tissue regeneration.

# 4.3 AI in Skin TE

Skin Tissue Engineering (STE) demands scaffolds capable of stimulating angiogenesis, supporting keratinocyte proliferation, and accelerating wound closure.  The AI assists in this process by directing the design and fabrication of bi-layered scaffold systems and predicting cell–matrix interactions that facilitate efficient tissue regeneration. Through data-driven modeling, AI can correlate scaffold architecture, surface chemistry, and biomolecule distribution with wound healing outcomes, thereby enabling the creation of tailored materials that mimic native skin structure and function.

## 4.3.1 Predicting Wound Healing and Cell Migration

AI-driven predictive frameworks can replicate the temporal dynamics of wound healing by modeling key biological events such as cell migration, proliferation, and Extracellular Matrix (ECM) remodelling. Leveraging datasets derived from in vitro wound closure assays, Long Short-Term Memory (LSTM) neural networks have been employed to forecast healing trajectories based on scaffold porosity, degradation rate, and cytokine release profiles (Kim et al., 2021). This predictive capability facilitates the rational design of personalized scaffolds, particularly beneficial for patients with chronic wounds or diabetic ulcers where normal regenerative mechanisms are compromised.

## 4.3.2 Image-Based Scaffold Quality Assessment

High-resolution imaging combined with CNN algorithms enables automated characterization of skin scaffold morphology, fiber orientation, and pore distribution. In a study by Mousavi et al. (2023), AI-assisted image analysis of electrospun collagen scaffolds successfully identified key structural parameters that enhanced fibroblast adhesion, achieving 94% accuracy relative to manual expert assessment. This image-driven evaluation approach strengthens quality control and promotes reproducibility—both of which are critical for the clinical translation of engineered skin substitutes.

# 4.4 AI in Vascular TE

Vascularization remains one of the primary challenges in tissue engineering, as effective tissue regeneration relies on adequate oxygen and nutrient transport. The AI plays a pivotal role in addressing this limitation by enabling the computational design of perfusable vascular scaffolds that promote endothelialization and optimize fluid dynamics within the construct.

## 4.4.1 Computational Hemodynamics with AI

Deep learning algorithms can simulate fluid flow and shear stress within microvascular networks with greater efficiency than conventional Computational Fluid Dynamics (CFD) methods. Khan et al. (2022) developed a CNN–based surrogate model capable of predicting flow distribution in branched vascular scaffolds, achieving computational speeds up to 100 times faster than traditional CFD simulations. This acceleration facilitates iterative optimization of microchannel geometries, ensuring uniform perfusion and minimizing hypoxic zones within engineered tissues.

## 4.4.2 Endothelial Cell Response Prediction

The AI models have also been employed to predict endothelial cell adhesion, migration, and tube formation as functions of scaffold stiffness and surface chemistry (Li et al., 2024). Random forest classifiers trained on in vitro angiogenesis datasets have accurately identified material parameters that enhance vascular network formation. When integrated with microfluidic fabrication systems, these predictive models enable automated adjustment of scaffold microenvironments, fostering optimal conditions for vascularization and tissue perfusion.

# 4.5 AI in Neural TE

Neural Tissue Engineering (NTE) focuses on developing scaffolds that support neuronal growth, synaptic connectivity, and axonal guidance. AI provides predictive tools for optimising both scaffold architecture and neurobiological responses.

## 4.5.1 Neural Network–Based Optimisation

Appropriately, the ANNs—which emulate the structure and function of biological neurons—have been utilised to model neuron–scaffold interactions. AI models trained on electrophysiological datasets and microtopographical parameters can predict neuron alignment, firing dynamics, and synaptic density (Huang et al., 2022). For example, Wu and Chen (2023) applied CNNs to analyse fluorescence microscopy images of neurons cultured on electrospun nanofibers, uncovering strong correlations between fiber orientation and neurite extension length. These findings provide valuable guidance for designing anisotropic scaffold architectures that promote directional axonal growth and functional neural regeneration.

## 4.5.2 Predictive Toxicity and Biocompatibility

In neural tissue engineering applications, material toxicity presents a major challenge. Machine Learning (ML) models have been employed to predict cytotoxicity and inflammatory responses based on polymer composition, surface modifications, and degradation by-products (Ahmed et al., 2021). Such predictive analytics enable early computational screening of candidate materials, significantly reducing reliance on extensive animal testing prior to in vivo evaluation. Furthermore, AI-guided material selection facilitates the optimization of scaffold formulations that balance mechanical flexibility with electrical conductivity—properties essential for neural prostheses and Brain–Machine Interface (BMI) systems. By integrating biocompatibility prediction with functional performance modeling, AI contributes to the development of safer and more effective neuro-regenerative scaffolds.

# 4.6 Cross-Disciplinary Integration and Translational Potential

The most transformative applications of AI in scaffold-based TE stem from multimodal data fusion and digital twin technologies. Digital twins—virtual, dynamic replicas of biological tissues—integrate real-time data from sensors, imaging modalities, and computational simulations to emulate scaffold behavior under physiological conditions (Li et al., 2024). These AI-driven digital twins enable predictive evaluation of cell proliferation, nutrient transport, and mechanical loading, thereby supporting pre-clinical optimization and personalized scaffold design. Additionally, federated learning frameworks facilitate collaborative AI model training across multiple research institutions without direct data exchange, effectively addressing issues of data privacy, reproducibility, and bias (Ma and Zhao, 2024). By leveraging distributed datasets and multimodal analytics, this paradigm enhances model generalizability and accelerates the translation of AI-guided scaffold innovations into real-world biomedical applications.

Table 4: Summary of AI Applications Across Tissue Types

| Tissue Type | AI Approach | Key Outcomes | Representative Study |
| --- | --- | --- | --- |
| Bone | ANN, FEA–AI Hybrid | Predict mechanical & degradation properties | Li et al. (2024) |
| Cartilage | SVR, CNN | Optimize stiffness & GAG production | Almalki and Alghamdi (2023) |
| Skin | LSTM, CNN | Predict wound healing & scaffold morphology | Kim et al. (2021) |
| Vascular | CNN, RF | Model flow dynamics & endothelialization | Khan et al. (2022) |
| Neural | ANN, CNN | Predict neuron alignment & scaffold biocompatibility | Wu and Chen (2023) |

AI has therefore evolved from a computational curiosity into a core enabler of next-generation scaffold design. Through the integration of predictive modeling, real-time fabrication control, and biological feedback, AI empowers researchers to engineer patient-specific, performance-optimized, and clinically translatable scaffolds across diverse tissue types. This convergence of intelligent algorithms with biomaterial science marks a paradigm shift from empirical scaffold development toward data-driven, adaptive, and precision-guided tissue engineering.

# 5. Challenges, Limitations and Future Prospects of AI-Driven Scaffold Design and Optimisation

# 5.1 Data-Related Challenges

One of the foremost challenges in integrating AI into scaffold optimisation lies in data availability and quality. High-performing AI models require large, diverse, and well-annotated datasets to achieve reliable and generalisable predictions (Mousavi et al., 2023). However, in tissue engineering, most datasets remain fragmented, heterogeneous and confined to small-scale experimental studies. Variations in scaffold fabrication techniques, biomaterial compositions and biological assay conditions often result in non-standardised data that hinder model generalisation (Ramesh et al., 2022). Moreover, experimental inconsistencies—including differences in cell culture protocols, donor tissue variability and measurement methodologies—introduce noise that obscures true biological relationships. The absence of open-access repositories for scaffold characterisation parameters such as pore morphology, degradation kinetics and biocompatibility indices, further constrains AI model training and benchmarking. In order to overcome these limitations, researchers advocate for standardised data-sharing frameworks guided by the  Findable, Accessible, Interoperable and Reusable (FAIR) data principles, which aims to enhance transparency, reproducibility and scalability in AI-driven TE (Huang et al., 2024).

# 5.2 Computational and Model-Based Limitations

Despite remarkable progress in computational technologies, training AI models for scaffold optimisation continues to demand significant computational resources. Deep learning structures such as CNNs and Generative Adversarial Networks (GANs) require substantial GPU or TPU processing capacity, which makes them less accessible to laboratories with limited computing infrastructure (Gupta and Singh, 2023).

Another major challenge concerns model interpretability. Many deep learning systems function as “black boxes,” producing predictions without revealing how input parameters contribute to the final outcomes (Kumar et al., 2022). This lack of transparency weakens scientific confidence and regulatory approval, particularly in biomedical research where interpretability and reproducibility  are essential. Recent progress in Explainable Artificial Intelligence (XAI) has demonstrated potential in visualizing feature importance and uncovering relationships between scaffold microstructure and cellular responses. Nevertheless, these interpretability methods remain under refinement and are not yet uniformly adopted across tissue engineering platforms (Zhao et al., 2024). Furthermore, overfitting continues to be a persistent concern, especially when datasets are limited or unbalanced. Overfitted models tend to perform exceptionally on training data yet fail to predict accurately when applied to new or different scaffold designs. The use of cross-validation, regularisation and transfer learning techniques can help alleviate this issue, but it often persists when biological complexity surpasses the model’s capacity to generalise.

# 5.3 Integration with Experimental and Clinical Validation

For AI-based scaffold optimisation to achieve real-world impact, its outcomes must progress beyond computational simulations to validate experimental and clinical performance. This transition necessitates comprehensive in vitro and in vivo verification, which can be both costly and time-intensive (Okonkwo et al., 2023). Bridging the gap between algorithmic design and biological functionality remains complex due to the multiscale nature of tissue regeneration, encompassing molecular interactions at the nanoscale and physiological integration at the organ level.

In many cases, AI-generated scaffold designs exhibit excellent theoretical performance but fail to maintain stability or function under biological or mechanical stress during experimental validation (Singh and Ramesh, 2023). The absence of standardised evaluation protocols for AI-optimised scaffolds further complicates comparisons between studies. Developing integrated frameworks that combine AI-based predictions with real-time bioprinting feedback and sensor-driven validation could enhance reproducibility and facilitate translation into clinical applications. Clinical implementation of AI-assisted scaffold technologies also encounters regulatory barriers. Medical devices embedded with AI components are subject to evolving policies from regulatory bodies such as the United States Food and Drug Administration (FDA) and the European Medicines Agency (EMA). These organisations demand transparent documentation of model development, data sources and decision-making logic—requirements that remain challenging to fulfill for complex deep learning systems characterised by limited interpretability (Wang et al., 2024).

# 5.4 Ethical and Security Considerations

AI-based biomedical design introduces important ethical, legal and privacy challenges that must be addressed to ensure responsible innovation. The creation of patient-specific scaffolds often depends on access to sensitive biomedical imaging data such as Magnetic Resonance Imaging (MRI) and CT scans. Therefore, strict adherence to privacy regulations including the General Data Protection Regulation (GDPR) and the Health Insurance Portability and Accountability Act (HIPAA) as well as the implementation of secure data management protocols, are essential (Almalki and Alghamdi, 2023).

Another major concern involves potential biases embedded within AI training datasets. Underrepresentation of specific tissue types or demographic groups can lead to inaccurate predictions and unfair clinical outcomes, undermining the equity and reliability of AI-assisted scaffold design. To counter these risks, comprehensive ethical frameworks emphasising transparency, accountability and inclusivity are needed during AI model development. Additionally, the increasing use of generative and autonomous AI systems in biomedical engineering raises complex questions about IP rights. It remains unclear whether ownership of AI-generated scaffold designs should be attributed to software developers, data contributors or clinical practitioners utilising the technology. Establishing clear ethical and legal guidelines will be critical as AI continues to advance and integrate into biomedical research and healthcare innovation (Thakur et al., 2022).

# 5.5 Technical and Manufacturing Barriers

As stated by Mohan et al. (2024), although AM technologies such as 3D bioprinting and electrospinning provide remarkable precision in scaffold fabrication, embedding AI control into these systems introduces considerable technical difficulties. The AI frameworks are required to interpret real-time sensor feedback, regulate extrusion flow, identify structural irregularities and automatically adjust parameters to preserve design accuracy. Nonetheless, most existing AM platforms do not possess the level of hardware–software compatibility necessary for such intelligent adaptability.

Similarly, Liu et al. (2023) explained that variations in material properties pose additional barriers to AI integration. Natural polymers such as collagen, gelatin and chitosan, as well as synthetic polymers like Polylactic Acid (PLA), Polycaprolactone (PCL), and Polyethylene Glycol (PEG), exhibit distinct rheological behaviours, making it difficult for AI systems to fine-tune processing parameters accurately. Furthermore, scaling up AI-driven manufacturing from laboratory experiments to full industrial production demands substantial infrastructural investment, enhanced automation and rigorous quality assurance to ensure consistency and compliance across batches.

# 6. Conclusion and Future Directions

The incorporation of AI into scaffold optimisation has transformed the field of TE by linking computational intelligence with biological systems. Through the combined application of machine learning, deep learning and evolutionary algorithms, AI has shown significant promise in improving scaffold design, forecasting biological responses and expediting experimental processes. This interdisciplinary integration enhances scaffold performance, while advancing the broader goal of personalised and precision-based TE.

# 6.1 Key Insights

In summary, while AI-driven scaffold optimisation offers transformative potential, its success depends on overcoming key barriers in data standardisation, model transparency, ethical governance and experimental translation. The convergence of AI, AM and regenerative biology heralds a new era of intelligent TE, where computational insights guide material design with unprecedented precision. AI-driven scaffold optimisation signifies a major transformation from conventional empirical approaches to data-oriented discovery in TE. According to Liu et al. (2023), machine learning algorithms such as SVM, random forests and gradient boosting methods have been effectively utilised to establish correlations between material attributes and cellular responses, enabling accurate prediction of scaffold performance. Deep learning approaches, particularly CNNs have improved image-based assessments of scaffold microarchitecture, providing detailed insights into porosity, surface morphology, and degradation dynamics that directly influence tissue regeneration. Furthermore, evolutionary algorithms including genetic algorithms and particle swarm optimisation, have advanced multi-objective design by optimizing mechanical strength, biocompatibility, and biodegradability simultaneously (Zhang et al., 2024). Collectively, these AI frameworks enable iterative refinement of scaffold design, improving efficiency, reproducibility, and scalability.The integration of AI has expanded understanding across critical domains of tissue engineering, including microstructural control, biomaterial selection, in silico modeling, and AM. By analysing extensive experimental datasets, AI systems can autonomously predict optimal scaffold parameters and fabricate constructs suited for specific tissues such as bone, cartilage and neural networks. This data-guided approach reduces dependence on trial-and-error experimentation and accelerates clinical translation of novel biomaterials. Future progress will rely on multidisciplinary collaboration among engineers, data scientists, biologists and clinicians to ensure that AI becomes a reliable partner in regenerative healthcare.

# 6.2 Existing Barriers and Considerations

Despite its transformative potential, AI-assisted scaffold optimisation faces significant challenges that hinder widespread adoption. As noted by Ramesh et al. (2022), a lack of standardised, high-quality datasets limits the generalisability of many AI models. Data fragmentation across studies and differences in fabrication methods, material properties and biological assays often lead to inconsistent outcomes. Additionally, limited collaboration between data scientists and biomedical engineers restricts the development of multidisciplinary frameworks.  Ethical, legal and regulatory issues present further obstacles. The opaque nature of deep learning models often reduces interpretability, raising concerns regarding clinical accountability and trust (Kumar et al., 2022). Patient-specific modelling also introduces data privacy challenges, requiring strict adherence to frameworks such as the GDPR and HIPAA. Without transparent and explainable AI systems, regulatory approval processes remain complex and slow. Another major barrier is the limited interoperability between hardware and software systems. Current three-dimensional bioprinting platforms often operate in closed environments, restricting integration with AI algorithms that depend on live sensor feedback and adaptive learning. According to Mohan et al. (2024), developing open-source bioprinting architectures will be essential to achieve adaptive manufacturing guided by AI-driven predictions and real-time imaging data.

# 6.3 Future Directions

A research by Zhang et al. (2024) highlighted that despite existing challenges, the future of AI-integrated scaffold optimisation remains highly promising. The study reported a growing trend toward the use of multimodal AI models that combine imaging, mechanical and biological data to achieve a more holistic assessment of scaffold performance. These integrated models demonstrate superior accuracy in linking morphological characteristics, such as pore geometry, with biological outcomes like cell viability compared to conventional single-domain approaches. Nguyen et al. (2023) emphasised that federated learning represents another transformative approach, allowing decentralised AI model training across multiple research institutions, while maintaining data confidentiality. This method enables the creation of globally applicable scaffold optimisation frameworks trained on diverse datasets, thereby improving model generalisation, reproducibility, and clinical relevance.

Furthermore, Rahman et al. (2024) noted that the integration of AI-assisted bioprinting with real-time imaging and robotic feedback mechanisms will support the fabrication of patient-specific and anatomically precise scaffolds. The combination of AI and quantum computing may further accelerate the discovery process by enabling ultrafast simulations of material–cell interactions. Looking ahead, incorporating bioinformatics, systems biology and multi-omics data into AI-driven scaffold design could produce predictive models that connect scaffold characteristics to gene expression and regenerative outcomes. This interdisciplinary advancement would mark a significant step toward personalised regenerative medicine, where scaffold development is tailored to both tissue type and individual patient physiology.

Future research in AI-driven scaffold optimisation must prioritise multimodal and integrative approaches. As stated by Nguyen et al. (2023), combining imaging, biomechanics, genomics and transcriptomics data into unified AI models will allow a more comprehensive understanding of tissue–material interactions. Federated learning frameworks are expected to play a vital role by allowing cross-institutional training without compromising data confidentiality, leading to more robust and generalisable AI systems. Explainable AI (XAI) should also be prioritised to enhance model transparency and foster clinical trust. By visualising feature importance and mapping decision pathways, XAI can clarify how scaffold characteristics such as pore geometry or surface texture influence biological performance (Zhao et al., 2024). In addition, integrating AI with real-time bioprinting technologies will enable intelligent manufacturing processes. With embedded sensors and closed-loop feedback systems, AI can monitor and regulate printing parameters to maintain design fidelity and functional performance. This aligns with the development of digital twins—virtual biological replicas that simulate scaffold behavior and predict tissue responses before physical validation (Hosseini et al., 2022).

Emerging convergence between AI and omics sciences—such as proteomics, metabolomics, and transcriptomics—will provide deeper biological understanding, allowing scaffold designs to be fine-tuned based on molecular responses including gene expression and protein synthesis (Rahman et al., 2024). Such advancements will usher in the era of personalised regenerative medicine, where scaffold design is customised to each patient’s genetic and physiological profile. Long-term success will depend on building collaborative networks that connect biomedical engineers, material scientists, computer scientists and clinicians. The establishment of open-access databases, standardised metadata formats and reproducible methodologies will be fundamental in advancing innovation and accelerating translation into clinical practice.

# 6.4 Takeaway Remarks

In conclusion, the application of AI in scaffold optimisation represents a defining milestone in modern TE. By merging computational modelling with biological understanding, researchers can now create scaffolds that better mimic native tissue environments and support regenerative processes. Although challenges remain in data quality, interpretability and regulatory compliance, current research trajectories suggest a future where AI-enabled design and fabrication become the foundation of regenerative medicine. The ultimate objective is the realisation of fully automated, patient-specific systems that continuously adapt to biological feedback, producing advanced scaffolds that enhance healing, reduce rejection risks and improve clinical success rates. The continued evolution of this interdisciplinary field will fundamentally reshape the way regenerative therapies are developed and applied in contemporary biomedical science.

# COMPETING INTERESTS DISCLAIMER:

Authors have declared that they have no known competing financial interests OR non-financial interests OR personal relationships that could have appeared to influence the work reported in this paper.

# References

Ahmed, M., Ali, S., Rahman, K., & Chen, Y. (2024). Machine learning for dental tissue scaffold engineering. Frontiers in Cell and Developmental Biology, 12, 1497457.

Ahmed, N., Patel, S., & O’Connor, D. (2021). Machine learning models for predicting biodegradation kinetics of polymeric biomaterials. Journal of Biomedical Materials Research Part A, 109(7), 1456–1469.

Almalki, A., & Alghamdi, S. (2023). Machine learning approaches to optimize chondrogenic scaffold properties: A review. Biomedical Materials, 18(3), 032001.

Bagherpour, R., & Lee, J. (2025). Application of artificial intelligence in tissue engineering. Tissue Engineering Part B: Reviews, 31(1), 12–29.

Caforio, F., & Rossi, M. (2024). Physics-informed neural network estimation of material properties in soft tissue mechanics. Computational Mechanics, 64(5), 1231–1248.

Chen, C., Li, H., & Wu, J. (2023). Artificial intelligence in regenerative medicine: Opportunities and challenges. Trends in Biotechnology, 41(2), 145–158.

Chen, R., & Wang, L. (2022). Deep learning approaches for skin scaffold design. Frontiers in Bioengineering and Biotechnology, 10, 834611.

Fernández-García, R., Gómez, L., & Ortega, S. (2022). AI-guided neural scaffold optimization. Biomaterials Advances, 142, 213–226.

Gharibshahian, M., & Thompson, A. (2024). Recent advances in artificial intelligent strategies for tissue engineering: A review. Frontiers in Bioengineering and Biotechnology, 12, 11348508.

Ghosh, A., Patel, R., & Singh, M. (2022). Machine learning-assisted corneal scaffold development. International Journal of Artificial Organs, 45(4), 325–338.

Gupta, R., & Singh, P. (2023). Computational resource considerations for deep learning in biomaterials research. IEEE Access, 11, 54321–54336.

Gupta, S., & Lee, S. (2024). AI-driven vascular network scaffold design. Advanced Healthcare Materials, 13(6), 2400193.

Hollister, S. J. (2021). Porous scaffold design for tissue engineering using TPMS architectures. Advanced Healthcare Materials, 10(14), 2100456.

Hosseini, F., Rahman, S., & Kim, Y. (2022). Reinforcement learning for adaptive bioprinting control: Closed-loop parameter tuning. Biofabrication, 14(4), 045018.

Huang, L., Zhang, X., & Chen, Y. (2022). Machine learning and dynamic mechanical response prediction of tissue scaffolds. Journal of the Mechanical Behavior of Biomedical Materials, 135, 105458.

Huang, P., Zhao, J., & Lin, F. (2024). Generative adversarial networks for myogenic scaffold prediction. Acta Biomaterialia, 174, 155–169.

Jiang, F., Jiang, Y., Zhi, H., et al. (2017). Artificial intelligence in healthcare: Past, present and future. Stroke and Vascular Neurology, 2(4), 230–243.

Khan, N., Patel, R., & Zhao, L. (2022). CNN surrogate models for hemodynamics in vascular scaffolds. Computers in Biology and Medicine, 145, 105603.

Kim, S., Park, J., & Lee, H. (2021). LSTM models for wound healing prediction in skin scaffold studies. Journal of Tissue Engineering and Regenerative Medicine, 15(8), 629–641.

Kim, Y., & Zhao, L. (2023). Reinforcement learning for skeletal muscle scaffold control. IEEE Transactions on Neural Systems and Rehabilitation Engineering, 31(5), 1148–1161.

Kumar, A., & Singh, D. (2023). Evolutionary algorithms for multi-objective scaffold design optimization. Materials & Design, 225, 111360.

Kumar, R., & Singh, P. (2023). Bayesian optimization of bone scaffold geometry for multi-objective mechanical and biological performance. Journal of Biomedical Materials Research Part A, 111(4), 567–579.

Li, H., Wang, J., & Zhao, F. (2023). Support vector prediction of cartilage scaffold porosity for optimal regeneration. Biomedical Engineering Letters, 13(2), 213–228.

Li, X., Wang, T., & Zhao, Q. (2024). ANN-based prediction of mechanical properties in hydroxyapatite-polymer composites for bone scaffolds. Journal of Biomedical Materials Research Part B, 112(3), 445–459.

Limon, S. M., & Farid, A. (2024). Advancing scaffold porosity through a machine learning approach. Frontiers in Materials, 11, 1337485.

Liu, J., Wang, L., & Chen, M. (2022). Predictive modeling of dentin scaffold regeneration. Dental Materials, 38(9), 1125–1136.

Liu, Y., Zhang, H., & Liu, J. (2023). AI-assisted scaffold microarchitecture analysis using CNNs. Materials Today Bio, 15, 100403.

Ma, X., & Zhao, Y. (2024). Physics-informed neural networks (PINNs) for biodegradation modeling in biomaterials. Applied Mathematical Modelling, 115, 277–292.

Ma, X., Zhao, Y., & Liu, Z. (2021). Machine learning-assisted prediction of polymer scaffold degradation for tissue engineering. Journal of Biomedical Materials Research Part A, 109(5), 900–912.

Martins, D., Pereira, C., & Silva, P. (2023). AI in ocular tissue engineering. Journal of Tissue Engineering and Regenerative Medicine, 17(1), 102–116.

Mohan, R., Gupta, S., & Chen, L. (2024). AI-driven adaptive control in 3D bioprinting for scaffold fidelity. Additive Manufacturing, 66, 103561.

Mousavi, P., Santos, D., & Lee, M. (2023). Automated image-based classification of scaffold microstructure using deep learning. Journal of Microscopy, 289(2), 142–156.

Murphy, S. V., & Atala, A. (2020). 3D bioprinting of tissues and organs. Nature Biotechnology, 32(8), 773–785.

Nguyen, T., Tran, H., & Le, Q. (2023). Federated learning in healthcare: Enabling collaborative model training for biomedical applications. IEEE Journal of Biomedical and Health Informatics, 27(9), 4532–4542.

Okonkwo, U., Silva, J., & Roberts, B. (2023). Translational challenges for AI-designed scaffolds: In vitro to in vivo gaps. Regenerative Medicine, 18(5), 357–372.

Oladimeji, T., Adebayo, F., & Chen, S. (2024). Artificial intelligence in skin tissue engineering: Current progress and future prospects. Nanomaterials, 15(12), 895.

Paris, M., Rossi, F., & Bianchi, G. (2019). Curvature-driven growth mechanics in bone tissue engineering scaffolds: An in vivo study. Acta Biomaterialia, 90, 404–417.

Park, J., Choi, D., & Lee, H. (2023). Neural scaffold design using deep generative models. Tissue Engineering Part B: Reviews, 29(1), 15–29.

Patel, S., Huang, Y., & Zhao, L. (2022). Machine learning for predicting cartilage scaffold behavior. Materials Science and Engineering C, 134, 112646.

Piotrowska, U., & Kowalski, P. (2025). 3D bioprinting and artificial intelligence for tumor modeling and regenerative constructs. Cancers, 17(3), 2052.

Rahman, M., & Ahmed, S. (2024). Quantum computing prospects for material simulation in bioengineering. Journal of Computational Biology, 31(6), 611–627.

Ramesh, K., & D’Souza, P. (2022). Data standardization and reproducibility issues in tissue engineering research. Science and Technology of Advanced Materials, 23(1), 17–29.

Ren, Z., & Patel, N. (2025). Physics-informed neural networks: A comprehensive review. Applied Sciences, 15(14), 8092.

Roberts, S. J., Howard, D., Buttery, L. D., & Shakesheff, K. M. (2008). Clinical applications of musculoskeletal tissue engineering. British Medical Bulletin, 86(1), 7–22. https://doi.org/10.1093/bmb/ldn016

Sadée, C., & Moreno, P. (2025). Medical digital twins: Enabling precision medicine and personalized therapies. The Lancet Digital Health, 7(2), e120–e131.

Sel, K., & Martin, G. (2023). PINNs for physiological time series: Opportunities and limitations. npj Digital Medicine, 6, 153.

Shen, S., & Thompson, R. (2025). From virtual to reality: Digital twins in tumor therapy and scaffold assessment. Journal of Translational Medicine, 23, 371.

Singh, R., & Ramesh, P. (2023). Genetic algorithm optimization of porous scaffolds for load-bearing tissues. Materials Science and Engineering C, 138, 112654.

Sun, W., & Lee, J. (2024). Reinforcement learning for adaptive bioprinting strategies. IEEE Transactions on Biomedical Engineering, 71(5), 1256–1266.

Topol, E. J. (2019). High-performance medicine: The convergence of human and artificial intelligence. Nature Medicine, 25(1), 44–56.

Vallée, A., & Martin, L. (2025). Digital twins for personalized medicine: Requirements and standards. Journal of Medical Internet Research, 27(1), e72411.

Wang, T., Chen, Q., & Zhao, Y. (2023). Multi-objective AI optimization for vascular scaffold bioprinting. Biofabrication, 15(2), 025017.

Wang, Y., & Chen, M. (2023). Explainable AI approaches in biomedical materials: Visualizing feature importance in scaffold predictions. IEEE Transactions on Neural Networks and Learning Systems, 34(8), 4021–4033.

Wu, Y., & Chen, T. (2024). Harnessing the power of machine learning into tissue engineering: State, methods, and future trends. Frontiers in Bioengineering and Biotechnology, 12, 11630859.

Xu, H., & Li, F. (2023). Convolutional neural networks for μCT-based scaffold microstructure analysis. Journal of Materials Science: Materials in Medicine, 34(11), 89.

Yu, J., & Park, S. (2025). Machine learning in predicting and optimizing polymer bioink printability. Polymers, 17(2), 224.

Zhang, T., Wang, P., & Huang, R. (2022). Hybrid AI models for scaffold architecture optimization in tissue engineering. Computers in Biology and Medicine, 146, 105603.

Zhang, Y., Chen, Z., & Li, M. (2024). Deep learning-assisted 3D printing of bone tissue scaffolds. ACS Biomaterials Science & Engineering, 10(3), 1358–1371.

Zhang, Z., & Li, H. (2025). AI-driven 3D bioprinting for regenerative medicine: Systematic approaches. Biofabrication, 17(2), 2400505.

Zhao, B. R., & Lin, J. (2025). PINNs and inverse problems in biomaterials simulation. Neural Networks, 183, 345–360.

Zhao, Y., & Ma, X. (2024). Explainable AI and transparency in scaffold optimization. Materials Today Bio, 14, 100432.

Zhou, L., & Nguyen, H. (2022). ANN prediction of mesenchymal stem cell proliferation on polymer scaffolds. Biotechnology and Bioengineering, 119(6), 1540–1549.

Zhou, Y., Zhang, L., & Liu, X. (2022). Structural mechanics of lattice-based bone scaffolds: A review. Materials Today Bio, 15, 100312.