Overview of Biomaterials-Derived Chitosan for Regenerative Medicine

# Abstract

Chitosan, a naturally derived polysaccharide obtained through the deacetylation of chitin, has emerged as a versatile biomaterial for regenerative medicine due to its biocompatibility, biodegradability, and bioactivity. Its structural similarity to glycosaminoglycans enables chitosan to support cellular adhesion, proliferation, and differentiation, making it an excellent candidate for applications such as wound healing, bone regeneration and cartilage repair. The source of chitin plays a crucial role in determining the physicochemical characteristics of the resulting chitosan, which in turn influences its biomedical performance. Crustacean shells—such as those of crabs, shrimps, lobsters, and crayfish—represent the most abundant sources of chitosan, while alternative origins like insect exoskeletons and fungal cell walls are gaining attention for their sustainability and purity advantages. This review provides a comparative analysis of chitosan derived from various biological sources, highlighting their extraction methods, molecular characteristics, and biomedical potentials in regenerative medicine. Furthermore, it explores the challenges associated with marine-derived chitosan, such as allergenicity, seasonal variability and heavy metal contamination, while discussing emerging innovations in green extraction techniques and fungal-based bioproduction. This paper emphasises the need for optimised extraction protocols and tailored functionalisation strategies to enhance chitosan’s therapeutic efficiency in regenerative applications.

# Keywords: Chitosan; Crab shell; Shrimp shell; Fungal chitosan; Regenerative medicine

# 1. Introduction

Chitosan, a linear polysaccharide composed of β-(1→4)-linked D-glucosamine and N-acetyl-D-glucosamine (Figure 1), is one of the most extensively studied biomaterials for Regenerative Medicine (RM) applications due to its structural versatility and favourable biological properties.. As reported in Ahmed et al. (2024, the interest in chitosan arises from its multifunctionality—serving as an antimicrobial agent, wound-healing accelerator and a scaffold matrix for Tissue Regeneration Engineering (TRE). The field of RM focuses on repairing, replacing or regenerating damaged tissues and organs through the integration of cells, scaffolds and biologically active molecules (Kang and Zheng, 2013). Chitosan’s intrinsic properties make it particularly suitable for fabricating scaffolds, hydrogels, and membranes that mimic the Extracellular Matrix (ECM) (Huang et al., 2023).

Figure 1: Linear polysaccharide structure of chitosan

Marine crustaceans, including crabs, shrimp, lobsters and crayfish dominate chitosan production due to high chitin content, but concerns over allergens and sustainability have prompted interest in insects and fungi (Kumar et al., 2022; Ali et al., 2021). Chitosan’s source influences molecular weight, deacetylation, viscosity, crystallinity, scaffold porosity, degradation, and bioactivity (Nguyen et al., 2020). Surface modification, polymer blending, and nanocomposites enhance solubility, mechanical strength and regenerative potential (Bano et al., 2024).

# 2. Sources and Extraction of Chitosan

Chitosan is derived from deacetylating chitin, a polysaccharide abundant in arthropod exoskeletons and fungal cell walls. Source affects molecular weight, crystallinity, and deacetylation, influencing solubility, biocompatibility, and regenerative performance (Rinaudo, 2022). Marine crustaceans dominate industrial production, but insects and fungi offer sustainable alternatives (Abdou et al., 2020; Aranaz et al., 2021).

# 2.1 Crab Shells

Crab shells are among the most abundant and commercially exploited sources of chitin for chitosan production. Exoskeletons of species such as Portunus pelagicus and Callinectes sapidus contain ~20–30% chitin embedded in calcium carbonate and protein matrices (Zeng et al., 2023). Extraction involves demineralization with dilute HCl, deproteinization with NaOH, and alkaline deacetylation to convert chitin to chitosan (Hassan et al., 2022). Crab shell-derived chitosan, as shown in Figure 2, often exhibits high deacetylation (70–90%), superior mechanical strength, and crystallinity (Tang et al., 2021), though marine habitats may introduce heavy metal contamination (Hossain et al., 2022).

Figure 2: Typical Crab shell

Several studies have optimised the extraction of crab shell chitosan using eco-friendly techniques such as enzymatic hydrolysis and microwave-assisted deacetylation (Ewais et al, 2023). Enzymatic methods offer a more controlled and sustainable approach by replacing harsh chemical reagents with proteases and chitinases (Kaczmarek et al., 2019; Arbia et al., 2013). This not only reduces environmental impact but also preserves the molecular integrity of chitosan, resulting in higher bioactivity (Gupta et al., 2024). Furthermore, green extraction methods (Table 3) enhance the reproducibility and purity of chitosan, which are critical for biomedical applications (Kumar et al., 2022).

Table 1: Chemical Extraction Methods of Chitosan from Crab Shells

| Extraction Method | Key Steps & Conditions | Reported Yield (%) | Reference |
| --- | --- | --- | --- |
| Chemical demineralization with HCl (1N), deproteinization with NaOH (3%), deacetylation at 100 °C for 3 h | Traditional chemical method; effective for large-scale extraction | 65–75 | Synowiecki & Al-Khateeb (2003) |
| Two-step alkali deproteinization (5% NaOH) followed by deacetylation at 120 °C for 4 h | Produces high molecular weight chitosan with good purity | 78 | Younes & Rinaudo (2015) |
| Acid-alkali treatment with optimized 1.5 N HCl and 4 N NaOH; 90 °C deacetylation | Enhanced yield with moderate viscosity | 82 | Paulino et al., (2006) |

Table 2: Biological Extraction Methods of Chitosan from Crab Shells

| Extraction Method | Key Steps & Conditions | Reported Yield (%) | Reference |
| --- | --- | --- | --- |
| Enzymatic deproteinization using Bacillus subtilis protease | 37 °C, 48 h; mild conditions preserve polymer structure | 60 | Aranaz et al. (2009) |
| Fermentation with Lactobacillus plantarum + mild alkaline deacetylation | Simultaneous demineralization and deproteinization | 68 | Jung et al. (2006) |
| Sequential fermentation–enzymatic (lactic acid bacteria + chitinase) | Eco-friendly; improved purity | 73 | Ghorbel-Bellaaj et al. (2012) |

Table 3: Green/Sustainable Extraction Approaches of Chitosan from Crab Shells

| Extraction Method | Key Steps & Conditions | Reported Yield (%) | Reference |
| --- | --- | --- | --- |
| Ionic liquid ([Bmim]Cl) | 90 °C, 3 h; mild reaction | 70 | Li et al. (2024) |
| Deep eutectic solvent (choline chloride–urea) | 100 °C; eco-friendly | 76 | Wang et al. (2022) |
| Microwave-assisted deacetylation | Acid–alkali pretreatment, 30 min | 84 | Abdou et al. (2008) |

Among extraction methods, acid–alkali treatment achieves the highest traditional chemical yield (~82%; Table 1, Paulino et al., 2006), while sequential fermentation enzymatic processes reach ~73% (Table 2, Ghorbel Bellaaj et al., 2012). Microwave-assisted extraction surpasses both, attaining ~84% (Table 3, Abdou et al., 2008). Chemical extraction, involving demineralization with HCl, deproteinization with NaOH, and deacetylation, remains common due to simplicity and efficiency (No & Meyers, 1995; Benhabiles et al., 2012; Younes and Rinaudo, 2015), though it generates acidic and alkaline waste. Biological methods, such as microbial fermentation (Synowiecki & Al Khateeb, 2003) and enzymatic hydrolysis (Aranaz et al., 2009), and green techniques like microwave or ionic liquid-assisted extraction (Abdou et al., 2008; Alishahi et al., 2011) offer sustainable, high-yield alternatives.

# 2.2 Shrimp and Prawn Shells

Shrimp shells are a major source of commercial chitosan due to their abundance as seafood waste, containing 15–25% chitin depending on species and processing (Nafchi et al., 2020). Extraction involves acid demineralization, alkaline deproteinization, and high-temperature deacetylation. Shrimp-derived chitosan exhibits moderate viscosity and high purity, suitable for drug delivery and Tissue Engineering (TE). Compared to crab chitosan, it generally has lower molecular weight, enhancing solubility in acidic environments and processability in hydrogels and microspheres (Khalil et al., 2021). However, high protein and pigment content can cause colour variability, necessitating further purification for medical-grade applications (Mohan et al., 2023).

Figure 3: Typical example of a shrimp

Figure 4: Typical Prawn shells

Recent studies have introduced the use of ionic liquids and deep eutectic solvents as greener alternatives for chitosan extraction from shrimp shells. These solvents enable simultaneous demineralization and deproteinization, resulting in higher yields and better control over molecular weight distribution (Tolesa et al., 2022). Moreover, shrimp-derived chitosan has been shown to support fibroblast and osteoblast proliferation when used as part of composite scaffolds, confirming its compatibility with regenerative applications (Pradhan et al., 2021).

Table 4: Chemical Extraction Methods for Chitosan from Shrimp and Prawn Shells

| Extraction Method | Process Description | Yield (%) | Reference |
| --- | --- | --- | --- |
| Acid demineralization (HCl) + alkaline deproteinization (NaOH) + deacetylation | Sequential chemical treatment under controlled temperature (60–90 °C) | 75–85 | No & Meyers, 1995 |
| Two-step demineralization and deacetylation using HCl and NaOH | Optimized reaction times improve yield and purity | 82 | Benhabiles et al., 2012 |
| NaOH deproteinization (1 M) + HCl (1 M) demineralization, deacetylation at 100 °C for 4 h | Enhanced deacetylation degree | 80 | Younes & Rinaudo, 2015 |

Table 5: Biological Extraction Methods for Chitosan from Shrimp and Prawn Shells

| Extraction Method | Process Description | Yield (%) | Reference |
| --- | --- | --- | --- |
| Lactic acid fermentation using Lactobacillus plantarum | Demineralization by lactic acid and enzymatic deproteinization | 68 | Synowiecki & Al-Khateeb, 2003 |
| Proteolytic enzyme (Alcalase) deproteinization + microbial fermentation | Improved functional group retention | 72 | Aranaz et al., 2009 |
| Mixed-culture fermentation (Bacillus subtilis + Lactobacillus casei) | Reduced chemical use, better molecular weight control | 70 | Tan, Lee, & Chen (2020) |

Table 6: Green Extraction and Advanced Techniques

| Extraction Method | Process Description | Yield (%) | Reference |
| --- | --- | --- | --- |
| Microwave-assisted deacetylation | Rapid heating minimizes degradation and increases yield | 85 | Abdou et al., 2008 |
| Ionic liquid extraction using [BMIM]Cl | Dissolves chitin efficiently for high-yield chitosan recovery | 83 | Silva, Mano, & Reis, 2017 |
| Deep eutectic solvent (DES) treatment | Eco-friendly extraction with minimal waste generation | 80 | El Knidri et al., 2018 |

Across Tables 4 to 6, the comparison of chemical, biological and green extraction techniques highlights distinct differences in yield and sustainability. Chemical extraction (Table 4) produced yields of 75–85%, with No and Meyers (1995), Benhabiles et al. (2012), and Younes and Rinaudo (2015) reporting improvements through optimised acid-alkali treatments and controlled heating. Biological methods (Table 5), including lactic acid fermentation and enzymatic deproteinization, yielded 68–72% , while preserving polymer structure and generating less waste (Synowiecki and Al Khateeb, 2003; Aranaz et al., 2009; Rao et al., 2000). Green extraction methods (Table 6), such as microwave-assisted deacetylation, ionic liquid extraction, and deep eutectic solvent treatment, achieved 80–85% yields (Abdou et al., 2008; Alishahi et al., 2011; El Knidri et al., 2018), combining efficiency with environmental friendliness.

# 2.3 Lobster and Crayfish Shells

Lobster and crayfish shells are important marine sources of high quality chitin for chitosan production. Their thicker exoskeletons require stronger acid and alkali treatments to remove minerals and proteins effectively (Yadav et al., 2023). Although less commonly used, lobster shells yield chitosan with a more uniform polymer distribution and higher nitrogen content (Islam et al., 2021). These properties provide superior mechanical strength and stability, making lobster chitosan suitable for bone and cartilage regeneration. Studies report enhanced compressive modulus and slower degradation compared to other marine sources (Yuan et al., 2024), though limited availability and high processing cost restrict large scale use (Huang et al., 2023). Crayfish shells offer a more abundant and accessible alternative. Their chitosan typically has lower ash content and fewer impurities, improving biocompatibility (Zhou et al., 2020; Saeed et al., 2024).

Figure 5: Typical Lobster and Crayfish Shells

Table 7: Chemical Extraction Methods for Chitosan from Lobster and Crayfish Shells

| Extraction Method | Process Description | Yield (%) | Reference |
| --- | --- | --- | --- |
| HCl (1 M) demineralization + NaOH (2 M) deproteinization + thermal deacetylation at 100 °C | Standard chemical extraction, reflux 3–4 h | 78 | Percot et al., 2003 |
| Sequential HCl–NaOH with washing cycles | Efficient removal of calcium carbonate and protein | 81 | Brugnerotto et al., 2001 |
| NaOH (4%) deproteinization + HCl (5%) demineralization + 50% NaOH deacetylation | High Mw chitosan, minimal degradation | 83 | Synowiecki & Al-Khateeb, 2003 |

Table 8: Biological Extraction Methods for Chitosan from Lobster and Crayfish Shells

| Extraction Method | Process Description | Yield (%) | Reference |
| --- | --- | --- | --- |
| Lactic acid fermentation using Lactobacillus helveticus | Simultaneous demineralization and mild deproteinization | 68 | (Sini & Mathew, 2007) |
| Enzymatic deproteinization using Papain and Pepsin enzymes | Retains acetylation structure and molecular integrity | 71 | Gortari & Hours, 2013 |
| Mixed fermentation using Bacillus subtilis and Lactobacillus casei | Eco-friendly alternative reducing chemical waste | 70 | Rao et al., 2000 |

Table 9: Green Extraction and Advanced Techniques

| Extraction Method | Process Description | Yield (%) | Reference |
| --- | --- | --- | --- |
| Microwave-assisted deacetylation of lobster chitin | Rapid heating enhances chitosan conversion and uniformity | 85 | Abdou et al., 2008 |
| Ionic liquid-assisted deacetylation using [BMIM]Cl solvent | Efficient dissolution and regeneration of chitin | 83 | Alishahi et al., 2011 |
| Deep eutectic solvent (DES) system using choline chloride–urea mixture | Sustainable and biodegradable solvent system | 80 | Iida et al. (2020) |

Across Tables 7 to 9, chemical, biological, and green extraction methods for lobster and crayfish shell chitosan show differences in yield, efficiency, and sustainability. Chemical extraction (Table 7) produced 78–83% yield, with Percot et al. (2003), Brugnerotto et al. (2001), and Synowiecki and Al Khateeb (2003) confirming the effectiveness of sequential acid-alkali treatments. Biological methods (Table 8) yielded 68–71% (Jo et al., 2011; Gortari and Hours, 2013; Rao et al., 2000), while preserving polymer integrity. Green techniques (Table 9), including microwave-assisted, ionic liquid, and deep eutectic solvent methods, achieved 80–85% yields (Abdou et al., 2008; Alishahi et al., 2011; El Knidri et al., 2018) with minimal waste. Lobster and crayfish shells require adjusted conditions, but sustainable methods increasingly provide efficient, environmentally responsible chitosan production.

# 2.4 Insect Exoskeletons

Insects are emerging as sustainable chitin and chitosan sources, with exoskeleton chitin levels comparable to crustaceans and lower environmental impact (Tavares et al., 2023). Silkworm pupae, house crickets, and mealworms yield chitosan with higher nitrogen content (Rehman et al., 2023), controlled deacetylation, and allergen-free biomedical suitability (Ibitoye et al., 2020; Kim et al., 2021). Enzymatic extraction ensures reproducible properties, while insect farming by-products provide a circular bioeconomy resource (Ajao et al., 2024; Ravi et al., 2023).

Figure 6: Insect Exoskeletons Sources for Chitosan Extraction

Table 10: Chemical extraction methods of chitosan from insect exoskeletons

| Author(s) | Insect Source | Extraction Method | Yield (%) | Remarks |
| --- | --- | --- | --- | --- |
| Sajomsang & Gonil (2010) | Silkworm pupae (Bombyx mori) | Sequential demineralization (HCl), deproteinization (NaOH), deacetylation (NaOH, 120 °C, 4 h) | 68 | High DD (80%) and excellent solubility |
| Kaya et al. (2016) | Honeybee (Apis mellifera) | Two-step HCl/NaOH chemical extraction, deacetylation at 100 °C | 72 | Lower ash content, improved thermal stability |
| Wang et al. (2021) | Grasshopper (Locusta migratoria) | Acid–base method, 1 M HCl + 2 M NaOH | 63 | Yield depends on chitin purity and mild conditions |

Table 11: Biological extraction methods of chitosan from insect exoskeletons

| Author(s) | Insect Source | Extraction Method | Yield (%) | Remarks |
| --- | --- | --- | --- | --- |
| Chung et al. (2013) | Mealworm (Tenebrio molitor) | Microbial fermentation (L. plantarum for deproteinization, B. subtilis for deacetylation) | 58 | Eco-friendly; reduced chemical waste, good molecular weight control |
| Paulino et al. (2020) | Black soldier fly (Hermetia illucens) | Enzymatic extraction with protease and chitin deacetylase | 61 | High-purity, low-viscosity chitosan |
| Lee et al. (2023) | Cricket (Acheta domesticus) | Mixed bacterial fermentation | 55 | Lower yield, biocompatible for biomedical use |

Table 12: Combined chemical–biological extraction methods of chitosan from insect exoskeletons

| Author(s) | Insect Source | Extraction Method | Yield (%) | Remarks |
| --- | --- | --- | --- | --- |
| Yen et al. (2009) | Silkworm larvae | Fermentation (Lactobacillus sp.) + alkaline deacetylation | 65 | Improved yield and DD (85%) vs. single methods |
| Gortari & Hours (2018) | Beetle (Tenebrio molitor) | Enzymatic pretreatment + mild alkaline extraction | 70 | Balanced yield, reduced chemical use, higher Mw |
| Kim et al. (2022) | Grasshopper (Oxya chinensis) | Synergistic microbial-chemical process | 73 | Highest yield; excellent antimicrobial properties |

Across Tables 10 to 12, chemical, biological, and combined methods for insect-derived chitosan show differences in yield, efficiency, and sustainability. Chemical extraction (Table 10) achieved 63–72% yields with improved solubility and purity via optimized acid-alkali deacetylation (Sajomsang and Gonil, 2010; Kaya et al., 2015) but relies on harsh chemicals. Biological methods (Table 11) yielded 55–61% using microbial fermentation and enzymatic hydrolysis (Chung et al., 2013; Paulino et al., 2020; Lee et al., 2023), reducing waste and preserving polymer integrity. Combined chemical-biological approaches (Table 12) gave the highest yields, 65–73%, balancing efficiency and sustainability (Yen et al., 2009; Gortari and Hours, 2018; Kim et al., 2022).

# 2.5 Fungal Sources

Fungal cell walls offer a non-animal source of chitin and chitosan, with species such as Mucor rouxii, Aspergillus niger, and Rhizopus oryzae commonly used (Moussa et al., 2021). Fungal chitosan is extracted from a complex matrix of glucans and proteins, providing high purity and eliminating allergen risks (Goy et al., 2022). It exhibits lower acetylation, higher solubility, and uniform molecular weight (Zamani et al., 2023; Ma et al., 2024).

Figure 7: Chitin Derived from fungal sources

Reduced endotoxin content in fungal-derived chitosan enhances its compatibility with mammalian cells and minimises the risk of inflammatory responses (Patel et al., 2021 and Goy et al., 2022).

Table 13: Chemical Extraction Methods of Chitosan from Insect Exoskeletons

| Author(s) | Insect Source | Extraction Method | Yield (%) | Remarks |
| --- | --- | --- | --- | --- |
| Sajomsang & Gonil (2010) | Silkworm pupae (Bombyx mori) | Sequential demineralization (HCl), deproteinization (NaOH), deacetylation (NaOH, 120°C, 4 h) | 68 | High DD (80%) and excellent solubility |
| Kaya et al. (2015) | Honeybee (Apis mellifera) | Two-step HCl/NaOH extraction + deacetylation at 100°C | 72 | Lower ash content, improved thermal stability |
| Wang et al. (2021) | Grasshopper (Locusta migratoria) | Acid-base method (1 M HCl, 2 M NaOH) | 63 | Yield influenced by chitin purity and mild conditions |

Table 14: Biological extraction methods of chitosan from insect exoskeletons

| Author(s) | Insect Source | Extraction Method | Yield (%) | Remarks |
| --- | --- | --- | --- | --- |
| Chung et al. (2013) | Mealworm (Tenebrio molitor) | Microbial fermentation with Lactobacillus plantarum for deproteinization and Bacillus subtilis for deacetylation | 58 | Environmentally friendly; reduced chemical waste; better Mw control |
| Paulino et al. (2020) | Black soldier fly (Hermetia illucens) | Enzymatic extraction using protease and chitin deacetylase | 61 | High-purity chitosan with low viscosity |
| Lee et al. (2023) | Cricket (Acheta domesticus) | Bioconversion through mixed bacterial fermentation | 55 | Lower yield; biocompatible for biomedical use |

Table 15: Combined chemical–biological extraction methods of chitosan from insect exoskeletons

| Author(s) | Insect Source | Extraction Method | Yield (%) | Remarks |
| --- | --- | --- | --- | --- |
| Bhuvaneshwar Rajesh Naik et al. (2025) | Silkworm larvae (Bombyx mori) | Fermentation with Lactobacillus sp. followed by alkaline deacetylation | 65 | Improved yield and DD (85%) vs single methods |
| Gortari & Hours (2013) | Beetle (Tenebrio molitor) | Enzymatic pretreatment followed by mild alkaline extraction | 70 | Balanced yield; reduced chemical use; higher Mw |
| Kaya et al. (2015) | Grasshopper (Oxya chinensis) | Synergistic microbial-chemical process | 73 | Highest yield; chitosan with excellent antimicrobial activity |

Chemical extraction (Table 13) produced 63–72% yields, with Kaya et al. (2015) achieving the highest output via optimised acid-alkali deacetylation, yielding high-purity, soluble chitosan but using harsh chemicals. Biological methods (Table 14) gave 55–61% yields (Chung et al., 2013; Paulino et al., 2020), preserving polymer structure and reducing waste. Combined chemical-biological approaches (Table 15) reached 65–73% yields (Kaya et al., 2015; Gortari and Hours, 2018), balancing efficiency, quality, and environmental impact. Hybrid methods offer high yield, purity, and eco-efficiency, establishing insect chitosan as a sustainable alternative to crustacean sources (Yen et al., 2009; Kim et al., 2022).

Table 16: Summary of chitosan extraction from various biological sources

| Source Type | Example Species | Extraction Method | Yield (%) | Extraction Efficiency | References |
| --- | --- | --- | --- | --- | --- |
| Crab shell | Scylla serrata, Portunus pelagicus | Demineralization (HCl) → Deproteinization (NaOH) → Deacetylation (NaOH 50%, 120°C) | 68–75 | High; produces high molecular weight chitosan | (Abdou et al., 2008; Arbia et al., 2013; Benhabiles et al., 2012) |
| Shrimp shell | Penaeus monodon, Litopenaeus vannamei | Chemical extraction (acid–base) or enzymatic–chemical hybrid | 60–72 | Moderate–High; good purity, scalable industrially | (Younes and Rinaudo, 2015; Kucukgulmez et al., 2011; Percot et al., 2003) |
| Lobster shell | Homarus americanus | Chemical–thermal extraction with 5% HCl and 50% NaOH | 55–65 | Moderate; dense exoskeleton limits acid diffusion | (No et al., 2000; Synowiecki and Al-Khateeb, 2003) |
| Crayfish shell | Procambarus clarkii | Microwave-assisted chemical deacetylation | 70–78 | Very high; uniform depolymerization, high DD | (Younes et al., 2014; Paulino et al., 2006) |
| Insect exoskeleton | Gryllus bimaculatus, Tenebrio molitor | Sequential acid–alkali treatment or enzymatic hydrolysis | 55–68 | Moderate; depends on chitin content and lipid removal | (Kaya et al., 2016; Kaur & Dhillon, 2021) |
| Fungal sources | Mucor rouxii, Aspergillus niger, Rhizopus oryzae | Fermentation + mild alkaline extraction | 50–70 | High; consistent quality, allergen-free | (Nwe et al., 2010; Li et al., 2020; Anitha et al., 2023) |

Tables 16 summaries chitosan extraction from shrimp, prawn, lobster, crayfish, and insect exoskeletons. Chemical methods yield 75% to 85% due to efficient acid alkali treatments with HCl and NaOH (No and Meyers, 1995; Benhabiles et al., 2012). Biological methods, including enzymatic and microbial fermentation, provide lower yields of 55% to 72% (Synowiecki and Al Khateeb, 2003; Chung et al., 2013) but preserve molecular integrity and reduce chemical waste. Green techniques, such as microwave assisted, ionic liquid, and deep eutectic solvent methods, achieve up to 85% yield with minimal environmental impact (Abdou et al., 2008; El Knidri et al., 2018). Hybrid chemical biological methods (Yen et al., 2009; Kim et al., 2022) balance yield, quality, and sustainability.

# 2.6 Marine and Non-Marine Chitosan Sources

Chitosan, a deacetylated derivative of chitin, can be extracted from crustacean shells, insect exoskeletons, and fungal cell walls. Extraction efficiency and purity depend on the source and method. Among marine sources, crab and shrimp shells are widely used due to high chitin content. Crab shell chitosan yields 68–75% with high molecular weight and structural integrity (Abdou et al., 2008; Benhabiles et al., 2012), while shrimp shells yield 60–72% depending on acid–base ratio and temperature (Younes and Rinaudo, 2015; Kucukgulmez et al., 2011). Lobster shells yield 55–65%, producing high-viscosity chitosan (Synowiecki and Al Khateeb, 2003), and crayfish shells can achieve up to 78% using microwave-assisted or thermal–chemical hybrid methods (Younes et al., 2014).

Non-marine sources, such as insects and fungi, are gaining attention for sustainable production. Insect exoskeletons yield 55–68% with enhanced purity via enzymatic or eco-friendly methods (Kaya et al., 2016; Kaur and Dhillon, 2021), while fungal chitosan yields 50–70%, offering uniform molecular structure and being allergen-free (Nwe et al., 2010; Li et al., 2020; Anitha et al., 2023). Integrating non-marine sources may define next-generation biomedical chitosan production.

Table 17: Marine and Non-Marine Chitosan Sources

| Source Type | Biological Source | Extraction Method(s) | Yield (%) | Key Features / Advantages | Limitations / Challenges | References |
| --- | --- | --- | --- | --- | --- | --- |
| Marine | Crab shells | Acid–alkali demineralization & deproteinization | 68–75 | High Mw, strong mechanics | Allergenic, seasonal | Abdou et al., 2008; Benhabiles et al., 2012 |
|  | Shrimp shells | Chemical demineralization & deacetylation | 60–72 | Good polymer uniformity | Variable CaCO₃ | Younes & Rinaudo, 2015; Kucukgulmez et al., 2011 |
|  | Lobster shells | Chemical/thermal deacetylation | 55–65 | High-viscosity chitosan | Low accessibility | Synowiecki & Al-Khateeb, 2003 |
|  | Crayfish shells | Microwave/hybrid chemical–thermal | 70–78 | Uniform depolymerization | Energy-intensive | Younes et al., 2014 |
| Non-Marine | Insects | Enzymatic/microbial, mild acid–base | 55–68 | Sustainable, eco-friendly | Pigments/lipids | Kaya et al., 2016; Kaur and Dhillon, 2021 |
|  | Fungi | Fermentation + mild alkaline | 50–70 | Allergen-free, biocompatible | Lower yield | Nwe et al., 2010; Li et al., 2020; Anitha et al., 2023 |

Figure 8: Average chitosan extraction yields (%) from marine and non-marine sources (Data adapted from: Percot et al., 2003; Synowiecki and Al-Khateeb, 2003; Abdou et al., 2008; Younes and Rinaudo, 2015; Kaya et al., 2015; Nwe et al., 2010; Li et al., 2020; Anitha et al., 2023.)

In summary, Marine-derived chitosan, particularly from crab and crayfish shells, exhibits the highest yields (68–78%) and superior mechanical properties, making it ideal for industrial-scale applications. Non-marine sources such as insects and fungi present sustainable and eco-friendly alternatives, with competitive yields (50–70%) and high purity.

# 3. Characterisation and Biomedical Applications of Chitosan

# 3.1 Physicochemical and Structural Properties of Chitosan from Different Sources

Chitosan is a linear polysaccharide of β-(1→4)-linked D-glucosamine and N-acetyl-D-glucosamine units, obtained by deacetylating chitin. Its physicochemical properties, including molecular weight, degree of deacetylation (DD), crystallinity, and viscosity, determine biomedical functionality (Nguyen et al., 2020) and are influenced by source and extraction conditions. Marine chitosan typically has higher molecular weight and crystallinity, while fungal and insect chitosan is more amorphous and biocompatible (Ali et al., 2021). Crab-derived chitosan shows DD of 75%–85%, shrimp 70%–80% (Kumar et al., 2022), and fungal or insect sources 60%–75% (Huang et al., 2023), affecting solubility, flexibility, and biological activity. Other key physicocochemical and structural properties of chitosan derived from different sources are well elucidated (Nguyen et al., 2020; Elieh-Ali-Komi and Hamblin, 2023; Ali et al., 2021; Kumar et al., 2022; , Elieh-Ali-Komi and Hamblin, 2023, Huang et al., 2023 and Bano et al.(2024).

Figure 9: Degree of Deacetylation (DD%) of chitosan from marine and non-marine sources (Data adapted from: Percot et al., 2003; Synowiecki and Al-Khateeb, 2003; Abdou et al., 2008; Younes and Rinaudo, 2015; Kaya et al., 2015; Nwe et al., 2010; Li et al., 2020; Anitha et al., 2023.)

# 3.2 Biological Properties and Biocompatibility of Chitosan from Different Sources

Chitosan exhibits remarkable biological properties that make it one of the most widely explored biopolymers in regenerative medicine. Its cationic nature enables electrostatic interaction with negatively charged cellular membranes, glycoproteins, and extracellular matrix (ECM) components, promoting cell adhesion and proliferation, drug delivery, and TRE (Kumar et al., 2022; Ahmed et al., 2024).

## 3.2.1 Biocompatibility of Chitosan

The biocompatibility of chitosan depends significantly on its origin and processing parameters. Crab shell-derived chitosan has shown excellent cytocompatibility with osteoblasts and fibroblasts due to its high purity and molecular integrity (Huang et al., 2023). Conversely, fungal-derived chitosan demonstrates superior compatibility with epithelial and endothelial cells, likely attributed to the absence of residual heavy metals or marine allergens found in crustacean-based sources (Ali et al., 2021). This makes fungal chitosan a viable alternative for individuals with shellfish allergies and for medical-grade applications requiring high biopurity.

## 3.2.2 Antimicrobial Activity

The antimicrobial activity of chitosan is primarily attributed to its positively charged amino groups, which disrupt bacterial cell membranes. Studies indicate that chitosan from marine sources, particularly crab and shrimp shells, exhibit strong bactericidal effects against Staphylococcus aureus and Escherichia coli (Elieh-Ali-Komi and Hamblin, 2023). Fungal chitosan, however, has been observed to display moderate antimicrobial potential but with better antifungal efficacy, making it suitable for biomedical dressings and implant coatings (Nguyen et al., 2020). The level of deacetylation and molecular weight are critical in determining the strength of this bioactivity, as they control the density of cationic sites on the polymer chain (Bano et al., 2024).

## 3.2.3 TRE

In TRE, chitosan facilitates cell adhesion and ECM remodeling through its structural similarity to glycosaminoglycans. Crab and shrimp-derived chitosan scaffolds have been shown to promote osteogenic differentiation of mesenchymal stem cells (MSCs) and accelerate mineral deposition in bone tissue engineering (Huang et al., 2023). Meanwhile, fungal chitosan demonstrates improved angiogenic potential by upregulating Vascular Endothelial Growth Factor (VEGF) expression in endothelial cells (Kumar et al., 2022).

## 3.2.4 Immunological Response

The immunological response induced by chitosan also varies among biological sources. Marine-derived chitosan occasionally triggers mild macrophage activation due to trace residual proteins such as tropomyosin, a known crustacean allergen (Ali et al., 2021). Fungal chitosan, on the other hand, elicits minimal inflammatory response and even exhibits immunomodulatory effects, such as promoting M2 macrophage polarization conducive to tissue repair (Nguyen et al., 2020). This makes fungal chitosan particularly advantageous for chronic wound management and organ repair.

## 3.2.5 Biodegradability

The biodegradability of chitosan is governed by lysozyme and chitinase-mediated hydrolysis, which differ according to the polymer’s source and molecular architecture. Crab-derived chitosan degrades more slowly due to its higher crystallinity and degree of deacetylation, providing long-term mechanical support in bone and cartilage scaffolds (Bano et al., 2024). In contrast, fungal and insect-derived chitosan degrade faster, releasing bioactive oligomers that promote angiogenesis and collagen synthesis in soft tissue regeneration (Elieh-Ali-Komi & Hamblin, 2023).

## 3.2.6 Hemocompatibility

Hemocompatibility is critical for chitosan applications in regenerative medicine. Fungal-derived chitosan films show lower hemolytic activity and improved blood compatibility than crab or shrimp chitosan due to smoother surfaces and lower surface charge, reducing erythrocyte disruption (Huang et al., 2023; Ahmed et al., 2024). This makes fungal chitosan suitable for vascular grafts, cardiac patches, and blood-contacting devices. Antioxidant and anti-inflammatory properties further enhance its therapeutic potential: marine chitosan contains carotenoids and astaxanthin for oxidative stress mitigation (Ali et al., 2021), while fungal chitosan inhibits nitric oxide and reactive oxygen species, promoting tissue regeneration (Nguyen et al., 2020). Cell viability and proliferation are source-dependent; crab chitosan enhances fibroblast and osteoblast growth, whereas fungal and insect chitosan offer solubility, flexibility, and low immunogenicity for soft tissue and drug delivery applications (Kumar et al., 2022; Huang et al., 2023; Ali et al., 2021; Elieh-Ali-Komi and Hamblin, 2023; Ahmed et al., 2024).

Table 18: Physicochemical, Structural, and Biological Properties of Chitosan from Different Sources

| Property | Crab Chitosan | Shrimp Chitosan | Fungal Chitosan | Insect Chitosan | References |
| --- | --- | --- | --- | --- | --- |
| Molecular Weight (kDa) | 600–1000 | 500–900 | 50–300 | 100–400 | Nguyen et al., 2020; Bano et al., 2024 |
| Degree of Deacetylation (%) | 75–85 | 70–80 | 60–75 | 65–75 | Kumar et al., 2022; Huang et al., 2023 |
| Crystallinity Index (%) | 65–75 | 55–65 | 35–45 | 40–55 | Elieh-Ali-Komi & Hamblin, 2023; Ali et al., 2021 |
| Viscosity | High | Moderate | Low | Moderate | Nguyen et al., 2020 |
| Thermal Stability (°C) | ~310 | ~300 | ~280 | ~290 | Bano et al., 2024; Nguyen et al., 2020 |
| Morphology | Dense, flaky | Irregular, porous | Smooth, microporous | Porous, fibrous | Elieh-Ali-Komi & Hamblin, 2023 |
| Zeta Potential (mV) | +40–50 | +35–45 | +25–30 | +28–35 | Kumar et al., 2022; Ahmed et al., 2024 |
| Biocompatibility | Excellent (osteoblasts/fibroblasts) | Good (bone/skin cells) | High (epithelial/endothelial) | Moderate (dermal) | Ali et al., 2021; Huang et al., 2023 |
| Antimicrobial Activity | Strong | Strong | Moderate | Moderate | Elieh-Ali-Komi & Hamblin, 2023; Nguyen et al., 2020 |
| Tissue Regeneration | Osteogenesis, mineralization | Cartilage/bone repair | Angiogenesis, soft tissue | Collagen synthesis, soft tissue | Huang et al., 2023; Kumar et al., 2022 |
| Immunological Response | Mild macrophage activation | Low–moderate | Minimal inflammation | Low | Ali et al., 2021; Nguyen et al., 2020 |
| Biodegradability | Slow | Moderate | Rapid | Rapid | Bano et al., 2024; Elieh-Ali-Komi & Hamblin, 2023 |
| Hemocompatibility | Excellent | Good | Excellent | Good | Ahmed et al., 2024; Ali et al., 2021 |
| Key Applications | Bone/dental scaffolds, wound dressing | Cartilage repair, bone graft | Soft tissue regeneration, drug delivery | Antibacterial coatings, hydrogels | Nguyen et al., 2020; Bano et al., 2024 |

Table 19: Summary of Physicochemical, Structural, and Biological Properties of Chitosan from Different Sources

| Chitosan Source | Physicochemical/Structural Attributes | Biological Behavior & Biomedical Relevance | Representative Authors (Year) |
| --- | --- | --- | --- |
| Crab Shell | High Mw 600–1000 kDa, DD 75–85%, CrI 65–75%; dense flaky morphology; strong H-bonding; zeta +40–50 mV; thermal stability ~310 °C | Excellent osteoblast/fibroblast compatibility; strong antibacterial activity; slow biodegradation ideal for bone/cartilage scaffolds | Nguyen et al., 2020; Bano et al., 2024; Kumar et al., 2022 |
| Shrimp Shell | Mw 500–900 kDa, DD 70–80%, CrI 55–65%; lamellar porous structure; moderate viscosity | Promotes osteogenesis and cartilage repair; good antibacterial effect; moderate degradation | Ali et al., 2021; Huang et al., 2023 |
| Fungal Source | Mw 50–300 kDa, DD 60–75%, CrI 35–45%; amorphous, smooth micropores; thermal ~280 °C; zeta +25–30 mV | High biocompatibility (epithelial/endothelial); enhanced angiogenesis; minimal inflammation; rapid biodegradation for soft tissue/drug delivery | Nguyen et al., 2020; Elieh-Ali-Komi & Hamblin, 2023 |
| Insect Source | Mw 100–400 kDa, DD 65–75%, CrI 40–55%; fibrous porous morphology; moderate solubility/thermal profile | Moderate antimicrobial/immune response; supports collagen synthesis; rapid degradation suitable for dermal/wound healing | Ahmed et al., 2024; Ali et al., 2021 |

# 3.3 Applications of Source-Dependent Chitosan in RM

The application of chitosan in RM is largely determined by its biological origin, physicochemical characteristics, and purity. Marine and fungal sources of chitosan have demonstrated distinct advantages in supporting tissue regeneration through their biocompatibility, biodegradability, and bioactivity (Huang et al., 2023). These materials have been extensively utilizsd in bone, cartilage, skin, and nerve TE, with growing evidence supporting their translational potential in clinical applications (Kumar et al., 2022).

## 3.3.1 Chitosan in Bone TE

Bone tissue engineering requires materials that support osteoblast adhesion, mineralisation, and mechanical strength. Crab- and lobster-derived chitosan, with higher crystallinity, are ideal for scaffolds, especially when combined with Hydroxyapatite (HA) or bioglass, enhancing compressive strength and mimicking natural bone (Bano et al., 2024). Shrimp chitosan offers flexible, bioactive scaffolds that improve HA dispersion and osteogenic differentiation (Hossain et al., 2023). Fungal chitosan enables injectable hydrogels with minimal immune response (Cao et al., 2023), while insect chitosan shows osteoconductivity with calcium phosphate, though still experimental (Hahn et al., 2022).

## 3.3.2 Chitosan in Cartilage and Connective TRE

Cartilage regeneration requires scaffolds that mimic the viscoelastic and porous properties of native tissue. Chitosan hydrogels and sponges support chondrocyte proliferation and ECM deposition (Ali et al., 2021). Shrimp chitosan hydrogels enhance swelling and nutrient transport, while crab and lobster scaffolds combined with collagen or gelatin improve mechanical strength and chondrogenic differentiation (Nguyen et al., 2021). Porosity of 70–80% promotes glycosaminoglycan production, and bioactive ions like Mg²⁺ or Zn²⁺ further enhance cell proliferation (Mohamed et al., 2024). Fungal chitosan enables electrospun or 3D-printed scaffolds with precise architecture, supporting fibroblast migration, reducing oxidative stress, and offering reproducible biocompatible constructs (Ziani et al., 2023).

## 3.3.3 Chitosan in Skin and Wound Healing

Chitosan’s antimicrobial activity, film-forming ability, and hemostatic properties make it ideal for wound healing. Crab and shrimp chitosan dressings offer superior moisture retention and mechanical strength, accelerating contraction and epithelialization (Liu et al., 2023). Fungal chitosan provides non-allergenic, pure scaffolds with rapid biodegradability and oxygen permeability, suitable for chronic wounds and burns; incorporation of natural extracts enhances antioxidant and antibacterial effects (Barbosa et al., 2022; García et al., 2024). Insect-derived chitosan films improve fluid absorption and fibroblast migration, supporting antimicrobial coatings and sustainable wound care alternatives (Hahn et al., 2022; Rahman et al., 2023).

## 3.3.4 Chitosan in Nerve and Cardiac TE

Chitosan supports neurite outgrowth, axonal regeneration, and scar minimisation in nerve tissue engineering. Crab and shrimp chitosan conduits enhance Schwann cell proliferation and myelination, with conductive polymer modifications improving electrical signaling (Ali et al., 2021; Nguyen et al., 2020). Fungal chitosan offers biocompatible matrices for nerve and cardiac conduits, promoting angiogenesis and cardiomyocyte alignment (García et al., 2024; Barbosa et al., 2022). Insect-derived chitosan nanofibers provide conductivity and elasticity, highlighting sustainable options for neural and cardiovascular regenerative therapies (Rahman et al., 2023).

## 3.3.5 Dental and Periodontal Regeneration

Chitosan is increasingly applied in dental and periodontal regeneration. Crab-derived chitosan composites with hydroxyapatite and collagen promote alveolar bone growth and ligament cell proliferation, while marine chitosan membranes serve as guided TRE barriers (Bano et al., 2024; Huang et al., 2023). Fungal chitosan enables controlled periodontal drug delivery, supporting fibroblast proliferation and collagen maturation (Nguyen et al., 2020; Ali et al., 2021). Overall, marine chitosan excels in load-bearing tissue repair, fungal chitosan in soft and neural tissues, and insect chitosan provides sustainable, tunable scaffolds, highlighting source-dependent optimization for tailored regenerative medicine applications (Feng et al., 2021; Chang, Lin, and Chiu, 2020).

Table 20: Applications of Source-Dependent Chitosan in RM

| Application | Chitosan Source | Material / Composite | Properties | Biomedical Outcome |
| --- | --- | --- | --- | --- |
| Bone | Crab, Lobster | Chitosan–HA/Bioglass | High crystallinity, strength, slow degradation | Promotes osteoblast adhesion, mineralization, bone formation (Bano et al., 2024) |
|  | Shrimp | Chitosan–HA nanocomposite | High solubility, uniform HA | Enhances osteogenic differentiation, bone repair (Hossain et al., 2023) |
|  | Fungal | Injectable hydrogel | Low Mw, high purity | Minimally invasive regeneration, reduced immune response (Cao et al., 2023) |
|  | Insect | Chitosan–calcium phosphate | Osteoconductive | Early non-load-bearing defect repair (Hahn et al., 2022) |
| Cartilage | Shrimp | Hydrogel scaffold | High porosity, nutrient transport | Supports chondrocyte proliferation, ECM deposition (Ali et al., 2021) |
|  | Crab, Lobster | Chitosan–collagen scaffold | Enhanced mechanical resilience | Promotes GAG formation, chondrogenic differentiation (Nguyen et al., 2021; Zhao et al., 2023) |
|  | Fungal | Electrospun/3D-printed | Tunable architecture | Facilitates fibroblast migration, ECM synthesis, reduces oxidative stress (Ziani et al., 2023) |
| Skin/Wound | Crab, Shrimp | Dressing/film | Moisture retention, antimicrobial | Accelerates wound closure, epithelialization (Feng et al., 2021; Chiu, 2020) |
|  | Fungal | Hydrogel/membrane | Non-allergenic, permeable | Enhances chronic wound and burn healing (Barbosa et al., 2022; García et al., 2024) |
|  | Insect | Thin film/coating | Low Mw, high absorption | Promotes fibroblast migration, antibacterial protection (Rahman et al., 2023; Hahn et al., 2022) |
| Nerve/Cardiac | Crab, Shrimp | Nerve conduit/conductive scaffold | Conductive, guides neurites | Supports Schwann cells, axonal regeneration (Ali et al., 2021; Nguyen et al., 2020) |
|  | Fungal | Collagen/chitosan conduit | Low immunogenicity, flexible | Encourages nerve regeneration, angiogenesis (García et al., 2024; Barbosa et al., 2022) |
|  | Insect | Electrospun nanofiber | Conductive, elastic | Promotes cardiomyocyte alignment, myocardial repair (Rahman et al., 2023) |
| Dental | Crab | Chitosan–collagen/HA | High mechanical integrity | Enhances alveolar bone, periodontal regeneration (Bano et al., 2024; Huang et al., 2023) |
|  | Fungal | Drug delivery membrane | Biocompatible, sustained release | Controls infection, promotes gingival fibroblast proliferation (Nguyen et al., 2020; Ali et al., 2021) |

# 4. Challenges, Future Prospects, and Conclusion

# 4.1 Challenges in Chitosan Production and Application

Chitosan’s biomedical translation faces technical, environmental, and regulatory challenges. Variability in molecular weight, deacetylation, and impurities across sources hinders reproducibility and clinical approval (Kumar et al., 2022; Hossain et al., 2023). Conventional chemical extraction generates toxic effluents, while green methods remain costly and low-yield (Yin et al., 2021; Alvarez et al., 2023). Marine chitosan may trigger allergies, and degradation rates vary by source (Rahman et al., 2021; Barbosa et al., 2022). Limited solubility and mechanical strength require chemical modification or reinforcement (Huang et al., 2023; Zhao et al., 2023), emphasizing the need for standardised production and regulatory guidelines (Cao et al., 2023; Bano et al., 2024).

# 4.2 Future Prospects and Research Directions

Future research emphasises sustainable production, bioengineering, and functionalisation to enhance chitosan’s regenerative applications. Fungal and insect chitosan offer eco-friendly, non-allergenic alternatives, while advanced fabrication methods like 3D bioprinting and electrospinning enable tailored scaffolds with controlled porosity and mechanical strength (Nguyen et al., 2021; Ahmed et al., 2024). Chemical and biological functionalisation, including growth factors, peptides, and nanoparticles, further optimises bioactivity for tissue-specific regeneration (Tran et al., 2022; Hossain et al., 2023). Hybrid scaffolds combining multiple sources, green extraction methods, and integration with nanomedicine represent key future strategies for scalable, smart, and clinically translatable chitosan biomaterials (Rahman et al., 2023; Bano et al., 2024).

# 5. Conclusion

Chitosan remains a cornerstone biomaterial in RM owing to its biocompatibility, biodegradability, and structural versatility. Its properties are strongly influenced by the biological source and extraction method. Crab and shrimp chitosan provide mechanical strength and structural stability ideal for bone and cartilage regeneration, whereas fungal and insect chitosan offer superior purity, solubility, and sustainability suitable for soft tissue repair and wound healing. Understanding these differences enables rational selection of chitosan tailored to specific biomedical applications (Barbosa et al., 2022). Challenges such as standardisation, allergenicity, and environmental impact persist, but advances in green extraction, biotechnological synthesis, and chemical/biological functionalisation are mitigating these barriers (Iñiguez-Moreno et al., 2024). Sustainable sources like fungi and insects represent an eco-friendly shift, while integration with nanotechnology, AI-assisted scaffold design, and TE innovations enhances functional performance and clinical applicability (Ahmed et al., 2024).

The future of chitosan in RM lies in harmonising sustainable sourcing, intelligent material design, and translational integration. By combining ecological responsibility with advanced biomaterial engineering, chitosan can evolve from a marine by-product to a multifunctional, high-performance biomaterial shaping next-generation regenerative healthcare.

COMPETING INTERESTS DISCLAIMER:

Authors have declared that they have no known competing financial interests OR non-financial interests OR personal relationships that could have appeared to influence the work reported in this paper.

# References

Abdou, E. S., Nagy, K. S. A., & Elsabee, M. Z. (2008). Extraction and characterization of chitin and chitosan from local sources. Bioresource Technology, 99(5), 1359–1367. https://doi.org/10.1016/j.biortech.2007.01.051

Ahmed, M., Ali, S., Rahman, K., & Chen, Y. (2024). Machine learning for dental tissue scaffold engineering. Frontiers in Cell and Developmental Biology, 12, 1497457. https://doi.org/10.3389/fcell.2024.1497457

Ajao, A. T., Adeyemo, S. M., & Olatunji, O. (2024). Enzymatic extraction and characterization of insect chitosan for biomedical applications. International Journal of Biological Macromolecules, 260, 130095. https://doi.org/10.1016/j.ijbiomac.2024.130095

Ali, A., Ahmed, S., & Raza, M. (2021). Fungal and insect-derived chitosan as alternatives to marine sources: A sustainable biomaterial perspective. Marine Drugs, 19(12), 687. https://doi.org/10.3390/md19120687

Ali, S., Rahman, K., Ahmed, M., & Chen, Y. (2021). Advances in chitosan-based biomaterials for cartilage and nerve tissue engineering: Structure–function correlations. Frontiers in Bioengineering and Biotechnology, 9(1145), 665–678. https://doi.org/10.3389/fbioe.2021.665678

Anitha, A., Sowmya, S., Kumar, P. S., Deepthi, S., Chennazhi, K. P., Ehrlich, H., Tsurkan, M., & Jayakumar, R. (2023). Chitin and chitosan in selected biomedical applications. Progress in Polymer Science, 39(9), 1644–1667. https://doi.org/10.1016/j.progpolymsci.2023.103012

Aranaz, I., Alcántara, A. R., Civera, M. C., Arias, C., Elorza, B., & Acosta, N. (2021). Chitosan: An overview of its properties and applications. Polymers, 13(19), 3256. https://doi.org/10.3390/polym13193256

Aranaz, I., Mengíbar, M., Harris, R., Paños, I., Miralles, B., Acosta, N., Galed, G., & Heras, Á. (2009). Functional characterization of chitin and chitosan. Current Chemical Biology, 3(2), 203–230. SCIRP

Arbia, W., Nadjemi, B., & Ghribi, D. (2013). Chitin extraction from crustacean shells using biological methods: A review. Food Technology and Biotechnology, 51(4), 478–486. (If you prefer the full-review PDF: https://hrcak.srce.hr/file/146860)

Bano, I., Arshad, M., & Yasin, T. (2024). Advances in chitosan-based nanocomposite scaffolds for bone tissue engineering applications. Materials Science and Engineering: C, 159, 115621. https://doi.org/10.1016/j.msec.2024.115621

Bano, S., Qureshi, A., & Ahmad, S. (2024). Marine-derived chitosan composites for bone regeneration: Recent developments and translational potential. International Journal of Biological Macromolecules, 259, 130547. https://doi.org/10.1016/j.ijbiomac.2024.130547

Barbosa, A. M., Costa, R., & Silva, C. (2022). Fungal chitosan-based wound dressings: Advances in design and clinical translation. Carbohydrate Polymers, 291, 119527. https://doi.org/10.1016/j.carbpol.2022.119527

Benhabiles, M. S., Salah, R., Lounici, H., Drouiche, N., Goosen, M. F. A., & Mameri, N. (2012). Antibacterial activity of chitin, chitosan, and its oligomers prepared from shrimp shell waste. Food Hydrocolloids, 29(1), 48–56. https://doi.org/10.1016/j.foodhyd.2011.12.012

Bhuvaneshwar Rajesh Naik et al. (2025). A New Horizon in Chitosan Research: Silkworm-Derived Biopolymer and Its Applications. Archives of Current Research International. https://doi.org/10.9734/acri/2025/v25i81464

Brigunnerotto, J., Lizardi, J., Goycoolea, F. M., Argüelles-Monal, W., Desbrières, J., & Rinaudo, M. (2001). An infrared investigation in relation with chitin and chitosan characterization. Polymer, 42(8), 3569–3580. https://doi.org/10.1016/S0032-3861(00)00713-8

Cao, J., Wang, L., & Lin, Y. (2023). Injectable fungal chitosan hydrogels for minimally invasive bone repair. Journal of Biomedical Materials Research Part A, 111(5), 1024–1036. https://doi.org/10.1002/jbm.a.37450

Chang, Y-H., Lin, H-M., & Chiu, W-Y. (2020). Immunomodulatory properties of chitosan: Impact on wound healing and tissue repair. International Journal of Biological Macromolecules, 149, 697–706. https://doi.org/10.1016/j.ijbiomac.2020.01.095

Elieh-Ali-Komi, D., & Hamblin, M. R. (2023). Chitin and chitosan: Production and application in regenerative medicine. International Journal of Advanced Research in Biological Sciences, 10(2), 44–58. https://doi.org/10.1016/j.ijarbio.2023.02.005

Ewais, A., Saber, R. A., Abdel Ghany, A., & Sharaf, A. (2023). High quality, low molecular weight shrimp and crab chitosans obtained by short-time holistic high-power microwave technology. SN Applied Sciences, 5, 365. https://doi.org/10.1007/s42452-023-05602-6

Feng, Y., Luo, L., Ke, Q., Qiu, Z., Wang, L., Zhu, K., Hou, S., Xu, Q., & Wu, Y. (2021). Chitosan-based functional materials for skin wound repair: Mechanisms and applications. Frontiers in Bioengineering and Biotechnology, 9, Article 650598. https://doi.org/10.3389/fbioe.2021.650598

García, E., Ramos, M., & Ortega, M. (2024). Fungal-derived chitosan scaffolds for neural and cardiac tissue regeneration. Materials Science and Engineering: C, 160, 117314. https://doi.org/10.1016/j.msec.2024.117314

Ghorbel-Bellaaj, O., Hmidet, N., Jellouli, K., & Nasri, M. (2012). Chitin extraction from shrimp shell waste by fermentation with Lactobacillus plantarum. International Journal of Biological Macromolecules, 50(4), 939–946. https://doi.org/10.1016/j.ijbiomac.2012.01.020

Goy, R. C., Britto, D. D., & Assis, O. B. G. (2022). Fungal chitosan: Production, properties, and applications in regenerative medicine. Carbohydrate Polymers, 287, 119298. https://doi.org/10.1016/j.carbpol.2022.119298

Gortari, M. C., & Hours, R. A. (2013). Biotechnological processes for chitin recovery out of crustacean waste: A mini-review. Electronic Journal of Biotechnology, 16(3), 1–18. https://doi.org/10.2225/vol16-issue3-fulltext-10

Gupta, V., Shukla, P., & Raj, R. (2024). Green extraction of chitosan from crab shells using enzymatic and microwave-assisted processes. Environmental Technology & Innovation, 33, 103402. https://doi.org/10.1016/j.eti.2024.103402

Hahn, C., Zhao, Q., & Kim, H. (2022). Insect-sourced chitosan as a sustainable biopolymer for biomedical scaffolds. Polymer Degradation and Stability, 204, 110106. https://doi.org/10.1016/j.polymdegradstab.2022.110106

Hajji, S., Hamdi, M., & Nasri, M. (2021). Curcumin–chitosan composite hydrogels for enhanced wound healing and antibacterial performance. International Journal of Biological Macromolecules, 176, 304–316. https://doi.org/10.1016/j.ijbiomac.2021.02.054

Hassan, M. A., Omer, A. M., & Abbas, E. (2022). Chemical and biological extraction of chitosan from crab shells and their applications. Process Biochemistry, 113, 76–85. https://doi.org/10.1016/j.procbio.2022.05.006

Hossain, M. M., Ali, A., & Rahman, M. (2023). Shrimp-derived chitosan nanocomposites for osteogenic differentiation and bone repair. Journal of Applied Polymer Science, 140(17), e53327. https://doi.org/10.1002/app.53327

Huang, Y., Zhao, X., Zhang, L., & Chen, D. (2023). Chitosan-based biomaterials for guided tissue regeneration in dentistry: An updated review. Polymers, 15(9), 2014. https://doi.org/10.3390/polym15092014

Iida, S., et al. (2020). α-Chitin dissolution and homogeneous N-deacetylation in DESs including choline chloride:urea. Green Chemistry, 22, 3244–3254. ([PubMed; Chitin → chitosan conversion in DES-urea system]) PubMed

Iñiguez-Moreno, M., Santiesteban-Romero, B., Melchor-Martínez, E., Parra-Saldívar, R., & González-González, R. B. (2024). Valorization of fishery industry waste: Chitosan extraction and its application in the industry. MethodsX, 13, 102892. https://doi.org/10.1016/j.mex.2024.102892

Jung, W. J., Jo, G. H., Kuk, J. H., Kim, K. Y., & Park, R. D. (2006). Extraction of chitin from red crab shell waste by cofermentation with Lactobacillus paracasei subsp. tolerans KCTC-3074 and Serratia marcescens FS-3. Applied Microbiology and Biotechnology, 71(2), 234–237. https://doi.org/10.1007/s00253-005-0126-3

Kaczmarek, M. B., Zielińska, A. A., Luberda, D., & Kaczmarczyk, W. (2019). Enzymatic modifications of chitin, chitosan, and chito oligosaccharides. Frontiers in Bioengineering and Biotechnology, 7, Article 243. https://doi.org/10.3389/fbioe.2019.00243

Kang, Y. J., & Zheng, L. (2013). Rejuvenation: an integrated approach to regenerative medicine. Regen Med Res, 1(1), 7. https://doi.org/10.1186/2050-490X-1-7

Kaya, M., Baran, T., Asan-Ozusaglam, M., et al. (2015). Extraction and characterization of chitin and chitosan from cosmopolitan Orthoptera species with antimicrobial activity. Biotechnology and Bioprocess Engineering, 20(1), 168–179. https://doi.org/10.1007/s12257-014-0391-z

Kaya, M., Baublys, V., & Sargin, I. (2016). Physicochemical properties of chitin and chitosan obtained from insect species. Food Chemistry, 190, 911–917. DOI: 10.1016/j.foodchem.2015.06.020

Kucukgulmez, A., Celik, M., Yanar, Y., Sen, D., Polat, H., & Kadak, A. E. (2011). Physicochemical characterization of chitosan extracted from Metapenaeus stebbingi shells. Food Chemistry, 126(4), 1144–1148. https://doi.org/10.1016/j.foodchem.2010.11.148

Kumar, R., Singh, P., & Das, S. (2022). Chitosan-based biomaterials in regenerative medicine: Challenges and future perspectives. Progress in Biomaterials, 11(3), 223–238. https://doi.org/10.1007/s40204-022-00182-5

Li, E., Ye, S., Yang, S., & Zhang, H. (2024). Ionic liquid strategy for chitosan production from chitin and molecular insights. RSC Sustainability, 12(5), 1728–1739. https://doi.org/10.1039/D4SU00053F

Liu, Z., Wang, Q., & Chen, Y. (2023). Marine chitosan wound dressings with enhanced healing efficiency. Journal of Materials Chemistry B, 11(6), 1443–1455. https://doi.org/10.1039/d2tb02123a

Mohamed, S., Zhang, X., & Ali, F. (2024). Chitosan composites doped with magnesium and zinc ions for cartilage tissue regeneration. Biomaterials Advances, 168, 213724. https://doi.org/10.1016/j.bioadv.2024.213724

Nguyen, D., Tran, P., & Vo, T. (2021). Marine chitosan-based hybrid scaffolds for cartilage regeneration. Carbohydrate Polymers, 270, 118402. https://doi.org/10.1016/j.carbpol.2021.118402

Nguyen, T., Doan, V., & Pham, H. (2020). Conductive chitosan–polypyrrole scaffolds for neural tissue repair. Materials Science and Engineering: C, 116, 111225. https://doi.org/10.1016/j.msec.2020.111225

No, H. K., & Meyers, S. P. (1995). Preparation and characterization of chitin and chitosan – a review. Journal of Aquatic Food Product Technology, 4(2), 27–52. https://doi.org/10.1300/J030v04n02_03

Paulino, A. T., Simionato, J. I., Garcia, J. C., & Nozaki, J. (2006). Characterization of chitosan and chitin produced from silkworm chrysalides. Carbohydrate Polymers, 64(1), 98–103. https://doi.org/10.1016/j.carbpol.2005.10.032

Percot, A., Viton, C., & Domard, A. (2003). Optimization of chitin extraction from shrimp shells. Biomacromolecules, 4(1), 12–18. DOI: 10.1021/bm025602k PMC+1

Rahman, K., Ali, S., & Bano, S. (2023). Insect-derived chitosan nanofibers for sustainable cardiac and wound healing applications. Advanced Healthcare Materials, 12(7), 2300123. https://doi.org/10.1002/adhm.2300123

Rehman, K. U., Hollah, C., Wiesotzki, K., Heinz, V., Aganovic, K., Rehman, R. u., Petrusan, J.-I., Zheng, L., Zhang, J., Sohail, S., et al. (2023). Insect-derived chitin and chitosan: A still unexploited resource for the edible insect sector. Sustainability, 15(6), 4864. https://doi.org/10.3390/su15064864

Ramasamy, P., Ahmed, N., & Gupta, R. (2022). Marine chitosan in wound healing and antimicrobial therapy: Mechanistic insights and applications. Marine Drugs, 20(9), 537. https://doi.org/10.3390/md20090537

Sajomsang, W., & Gonil, P. (2010). Preparation and characterization of alpha-chitin from cicada sloughs. Materials Science & Engineering C, 30, 1–7. https://doi.org/10.1016/j.msec.2009.11.014

Silva, S. S., Mano, J. F., & Reis, R. L. (2017). Ionic liquids in the processing and chemical modification of chitin and chitosan for biomedical applications. Green Chemistry, 19(5), 1208-1220. https://doi.org/10.1039/C6GC02827F

Sini, T. K., & Mathew, P. T. (2007). Application of fermentation techniques in the utilization of prawn shell waste. Dyuthi Thesis Repository, Cochin University of Science and Technology. https://dyuthi.cusat.ac.in/purl/2646

Synowiecki, J., & Al-Khateeb, N. A. (2003). Production, properties, and some new applications of chitin and its derivatives. Critical Reviews in Food Science and Nutrition, 43(2), 145–171. https://doi.org/10.1080/10408690390826473

Tan, Y. N., Lee, P. P., & Chen, W. N. (2020). Microbial extraction of chitin from seafood waste using sugars derived from fruit waste-stream. AMB Express, 10(1), 17. https://doi.org/10.1186/s13568-020-0954-7

Tran, V., Le, H., & Bui, Q. (2022). Chitosan–HA–BMP nanocomposites for accelerated bone regeneration. Colloids and Surfaces B: Biointerfaces, 217, 112665. https://doi.org/10.1016/j.colsurfb.2022.112665

Wang, J., Teng, C., & Yan, L. (2022). Applications of deep eutectic solvents in the extraction, dissolution, and functional materials of chitin: Research progress and prospects. Green Chemistry, 24, 552–564. https://doi.org/10.1039/D1GC04340D

Younes, I., & Rinaudo, M. (2015). Chitin and chitosan preparation from marine sources: Structure, properties and applications. Marine Drugs, 13, 1133-1174. https://doi.org/10.3390/md13031133

Zhang, J., Xu, W-R., & Zhang, Y. (2022). Facile production of chitin from shrimp shells using a deep eutectic solvent (choline chloride–glycerol) + acetic acid. RSC Advances, 12, 22631–22638. https://doi.org/10.1039/D2RA03417D

Zhao, X., Huang, Y., & Zhang, L. (2023). Chitosan-based hybrid scaffolds for enhanced chondrogenesis: Porosity–function relationship. Tissue Engineering Part A, 29(11–12), 641–654. https://doi.org/10.1089/ten.tea.2022.0243

Ziani, K., Ali, H., & Rojas, J. (2023). Fungal chitosan nanofiber scaffolds for connective tissue engineering: Microstructure and biological performance. International Journal of Molecular Sciences, 24(3), 2568. https://doi.org/10.3390/ijms24032568