Evaluation of Granule Size Indices in Commercially Available Urea Fertilizers in India

.

ABSTRACT

Urea is the most widely used nitrogen fertilizer in India, yet limited information is available on the granule size characteristics of commercially available products from different manufacturers. Granule size plays an important role in fertilizer handling, metering behavior, and field application uniformity. In the present study, urea samples were collected from ten major Indian manufacturers, and their particle size characteristics were evaluated using percentile-based granule size indices, including d5, d16, d84, and d90. The d5 values ranged from 0.394 to 0.861 mm, d16 ranged from 0.650 to 0.943 mm, d84 ranged from 1.311 to 1.484 mm, and d90 ranged from 1.359 to 1.565 mm. One-way ANOVA showed statistically significant differences (p < 0.05) for all granule size indices among the ten manufacturers, and Tukey post-hoc analysis indicated a high number of significantly different pairwise comparisons for each index. These findings highlight differences in size variability among Indian urea brands.

Keywords: Urea fertilizer, Granule size indices, Particle size distribution, Percentile diameters

1. INTRODUCTION

Nitrogen (N) is one of the most essential macronutrients required for plant growth and crop yield. Urea has emerged as the most widely used nitrogen fertilizer and serves as the primary nitrogen source in agricultural production systems (Bhatti, 1992; Glibert et al., 2006; M. K. Gamit et al., 2023). Urea accounts for over 50% of the nitrogen fertilizers utilized in the agricultural sector worldwide (Amiri et al., 2019). In India, the demand for urea has remained consistently high due to the country’s large agricultural sector and the extensive area under nitrogen-intensive crops such as rice and wheat. According to the recent governmental data, urea production in India increased from about 244.58 lakh metric tonnes per annum in 2019-20 to 314.09 lakh metric tonnes per annum in 2023-24 (Anonymous, 2024). Domestic production meets a large portion of the urea demand, with reports indicating that around 87.78% of urea consumption is currently met by indigenous manufacturing (Anonymous, 2024).

Despite this high production and use, there exist marked differences among commercially available urea fertilizers in terms of their physical properties. Particle size distribution is a key physical characteristic of granular fertilizers that affects their bulk behavior, including packing and segregation (Perfect et al., 1998). Among the factors affecting the deposition of granular fertilizers, particle size is the most significant, followed by particle density (Fulton & Port, 2016). The larger differences in particle size within a fertilizer increase the likelihood of uneven distribution or segregation (Gavrilović et al., 2018). Granule size influences various aspects of fertilizer performance, including flowability, bulk density, storage behaviour, spreading uniformity (for broadcast application), and discharge rate in mechanical or automated fertilizer applicators. One critical property is granule size distribution, often expressed through metrics such as d5, d16, d84, and d90 - indicating the diameters at which 5%, 16%, 84% and 90% of the sample’s mass falls below, respectively.   Uniformity and consistency in granule size distribution are particularly important when fertilizers are applied using precision or variable-rate application equipment, as uneven granule size may result in non-uniform discharge, misapplication, or blockages.

In recent years, the increasing adoption of mechanized, precision, and site-specific fertilizer application technologies has further highlighted the importance of detailed characterization of fertilizer granule size. Modern fertilizer spreaders and variable-rate applicators are highly sensitive to variations in granule size, as these directly influence spread pattern symmetry, application rate accuracy, and nutrient placement efficiency. Percentile-based granule size indices such as d5, d16, d84, and d90 provide a more robust description of the distribution extremes compared to single average size metrics, enabling better assessment of both fine and coarse fractions that govern segregation and discharge behaviour. Such detailed granulometric information is also essential for developing reliable uniformity indices, calibrating fertilizer metering mechanisms, and supporting particle-level numerical simulations used to predict fertilizer flow and spreading behaviour.

Internationally, several researchers have evaluated the particle size distribution and physical characteristics of granular fertilizers such as by Bhatti (1992), Miserque & Pirard, (2004), Rahmanian et al. (2015), Cousins et al. (2021), and Simsek & Guliyev (2021). Other work, such as that by Virk et al. (2013), obtained particle sizes (d16, d50, and d84) from the camsizer data. Shamsudin et al. (2014) investigated the influence of particle size on the direct compaction behavior of urea fertilizer. Although such research provides valuable insights into fertilizer performance at a global scale, studies focusing on the particle size characteristics of Indian urea fertilizers remain limited, despite India being one of the largest producers and consumers of urea globally. Variations in manufacturing technology, prilling versus granulation processes, and quality control practices among Indian manufacturers can lead to significant differences in granule size distribution, which in turn may influence fertilizer application uniformity. Although certain physical properties of fertilizers are commonly assessed during manufacturing, individual factories often use their own procedures to evaluate these characteristics (Allaire & Parent, 2004). However, actual particle sizes may differ from their intended specifications, as granules are susceptible to breakage and abrasion during transportation and handling. Therefore, the present study was undertaken to evaluate the particle size characteristics of ten commercially available urea fertilizer brands in India. Sieve analysis was conducted to determine the d5, d16, d84, and d90 indices, which serve as key descriptors of granule size distribution. The findings aim to provide insights into the physical quality of urea available in Indian markets and to support the design and calibration of fertilizer application systems.

2. material and methods

2.1 Sample Collection

Urea fertilizer samples were collected from ten different commercial brands commonly available in the Indian market. The manufacturers were selected based on their status as major urea producers in the country, considering factors such as production capacity, market presence, and distribution coverage. Together, these manufacturers represent a substantial portion of the commercial urea supply available to Indian farmers. A standard 45 kg bag of urea was procured from each manufacturer through authorized agricultural input suppliers and local fertilizer distribution outlets to ensure that the samples reflected the typical products available to end users. To maintain confidentiality, all collected samples were anonymized and labeled as Sample I, II, III, IV, V, VI, VII, VIII, IX, and X, with each designation corresponding to a distinct manufacturer widely represented in the Indian fertilizer market.

2.2 Sieve Analysis

In our previous work (Kumar et al., 2025), the sieve analysis procedure and the corresponding mass fraction retained on each sieve were described in detail to characterize the particle size distribution of commercial urea fertilizers. A schematic representation of the sieve stack arrangement is shown in Fig. 1. Sieve analysis was carried out in accordance with the standard procedure specified in ISO 8397:1988. From each ten samples, approximately 500 g of urea was placed on the top sieve, and the entire assembly was mounted on a mechanical sieve shaker for a fixed duration to ensure consistent vibration and complete separation of granules according to size. After sieving, the mass of material retained on each sieve was recorded, and the corresponding mass fraction was calculated. The percentage of material retained on a given sieve was determined using the equation 1 (Rutland, 1986). The present study employs these mass fraction data to compute percentile-based granule size indices, including d5, d16, d84, and d90. These indices enable a more detailed assessment of granule size variability by capturing both the finer and coarser fractions of the distribution, thereby providing deeper insights into the physical characteristics of urea fertilizers.

|  | Percentage retained on a sieve %=Mass retained on sieve (g)Total sample mass (g)×100 | …(1) |
| --- | --- | --- |

Fig. 1 Sieve Stack Arrangement

2.3 Determination of Granule Size Indices (Percentile Diameters d5, d16, d84, and d90)

The granule size indices of the urea samples were determined using percentile-based particle size parameters calculated from the cumulative mass distribution obtained through sieve analysis. For each sample, the cumulative percentage of material passing through successive sieves was plotted against the corresponding sieve aperture size to generate the particle size distribution curve. As described by Miserque & Pirard (2004), such curves are characterized by percentile diameters denoted as dx, where x represents the weight fraction (in percent) of particles passing a sieve of mesh size d.

Based on this principle, the percentile diameters d5, d16, d84, and d90 were determined by interpolation. The lower percentile diameters- d5 and d16-correspond to the particle sizes at which 5% and 16% of the sample mass passed through the sieve, indicating that the remaining 95% and 84% of the material, respectively, consisted of larger particles retained above that size. Conversely, the upper percentile diameters d84, and d90 represent the particle sizes below which 84% and 90% of the total sample mass passed, leaving 16% and 10% as the coarser fraction.

Together, these percentile-based parameters provide a detailed representation of the granule size distribution, capturing both fine and coarse components of the fertilizer samples. Their inclusion allows for a more comprehensive assessment of granule size variability than traditional single-point descriptors and offers deeper insight into the physical characteristics and handling behavior of commercially available urea fertilizers.

2.4 Statistical Analysis

The statistical analysis was conducted to evaluate the variability in the granule size indices of urea samples obtained from ten different manufacturers. Each sample was analyzed with four replications. A one-way analysis of variance (ANOVA) with Tukey’s post hoc test was performed to determine whether significant differences existed among the manufacturers for each of the granule size indices (d5, d16, d84, and d90). All statistical analyses were carried out using OriginPro 2025 (OriginLab Corporation, USA).

3. results and discussion

3.1 d5 Granule Size Index

The d5 values of the ten urea samples ranged from 0.394 mm to 0.861 mm, indicating notable variation in the smallest percentile diameter among the manufacturers. The coefficient of variation (CV) for d5 ranged from 0.12% to 4.95%, indicating differences in consistency within the individual samples. As illustrated in Fig. 2, the minimum d5 value was observed for Sample III, whereas the maximum d5 value was recorded for Sample IX.

The results of the one-way ANOVA, summarized in Table 1, demonstrated that the differences in the mean d5 values among the ten manufacturers were statistically significant at the 0.05 level. The Tukey post-hoc comparison further confirmed that 35 out of the 45 possible manufacturer pairings exhibited significant differences in d5 at the 0.05 significance level. These findings highlight the considerable variability in d5 among commercially available urea fertilizers, suggesting that manufacturers differ substantially in terms of granule size characteristics represented by this percentile diameter.

Fig. 2 d5 Granule Size Index for Urea Samples

Table 1: One-Way ANOVA for d5 Granule Size Index

| Source of Variation | DF | Sum of Squares | Mean Square | F Value | Tabular F (5%) |
| --- | --- | --- | --- | --- | --- |
| Model | 9 | 1.00215 | 0.11135 | 431.8819* | 2.21 |
| Error | 30 | 0.00773 | 2.57825E-4 |  |  |
| Total | 39 | 1.00988 |  |  |  |

3.2 d16 Granule Size Index

As shown in Fig. 3, the d16 values of the ten urea samples ranged from 0.650 mm (Sample III) to 0.943 mm (Sample IV), indicating variability in the lower percentile granule size among manufacturers. The CV for d16 varied from 0.00 to 1.06%. The results of the one-way ANOVA for d16 are presented in Table 2. The analysis showed that, at the 0.05 significance level, the differences in mean d16 values across the ten manufacturers were statistically significant. A subsequent Tukey post-hoc test further identified that 40 out of the 45 possible manufacturer pairwise comparisons exhibited significant differences at the 0.05 level, confirming substantial variability in d16 among the commercial urea brands.

Fig. 3 d16 Granule Size Index for Urea Samples

Table 2: One-Way ANOVA for d16 Granule Size Index

| Source of Variation | DF | Sum of Squares | Mean Square | F Value | Tabular F (5%) |
| --- | --- | --- | --- | --- | --- |
| Model | 9 | 0.24332 | 0.02704 | 1809.403* | 2.21 |
| Error | 30 | 4.4825E-4 | 1.49417E-5 |  |  |
| Total | 39 | 0.24377 |  |  |  |

3.3 d84 Granule Size Index

The d84 values of the ten urea samples ranged from 1.311 mm to 1.484 mm, indicating moderate variability among the manufacturers in the upper portion of the granule size distribution. The CV values for d84 were relatively low, ranging from 0.07% to 0.76%, suggesting that the larger granule fractions were generally consistent within each manufacturer's product. As illustrated in Fig. 4, the minimum d84 value was recorded for Sample III, whereas the maximum d84 value was observed for Sample IX.

The results of the one-way ANOVA for d84 presented in Table 3 showed that, at the 0.05 significance level, the differences in mean d84 values across the ten manufacturers were statistically significant, indicating non-uniformity in the coarser granule size characteristics among the brands. A subsequent Tukey post-hoc test revealed that 39 out of the 45 possible manufacturer pair comparisons exhibited significant differences at the 0.05 level. The high number of significant pairwise differences confirm substantial variability in the d84 granule size index among commercially available urea fertilizers in India.

Fig. 4 d84 Granule Size Index for Urea Samples

Table 3: One-Way ANOVA for d84 Granule Size Index

| Source of Variation | DF | Sum of Squares | Mean Square | F Value | Tabular F (5%) |
| --- | --- | --- | --- | --- | --- |
| Model | 9 | 0.09569 | 0.01063 | 484.206* | 2.21 |
| Error | 30 | 6.5875E-4 | 2.19583E-5 |  |  |
| Total | 39 | 0.09635 |  |  |  |

3.4 d90 Granule Size Index

As shown in Fig. 5, the d90 values of the ten urea samples ranged from 1.359 mm (Sample III) to 1.565 mm (Sample IX). The CV for d90 ranged from 0.00 to 0.63%, indicating relatively low within-manufacturer variability. The results of the one-way ANOVA for d90 are presented in Table 4. The analysis showed that, at the 0.05 significance level, the differences in mean d90 values across the ten manufacturers were statistically significant. A subsequent Tukey post-hoc test revealed that 40 out of the 45 possible manufacturer pairwise comparisons exhibited significant differences at the 0.05 level, indicating substantial variation in d90 among the commercially available urea brands.

Fig. 5 d90 Granule Size Index for Urea Samples

Table 4: One-Way ANOVA for d90 Granule Size Index

| Source of Variation | DF | Sum of Squares | Mean Square | F Value | Tabular F (5%) |
| --- | --- | --- | --- | --- | --- |
| Model | 9 | 0.19731 | 0.02192 | 924.708* | 2.21 |
| Error | 30 | 7.1125E-4 | 2.37083E-5 |  |  |
| Total | 39 | 0.19802 |  |  |  |

4. Summary and Conclusion

The present study evaluated the granule size characteristics of ten commercially available urea fertilizers in India using percentile-based indices (d5, d16, d84, and d90). The results highlighted substantial variability in particle size distribution among manufacturers, as revealed through one-way ANOVA and Tukey’s post hoc analysis. Such differences in granule size indices have important implications for fertilizer handling, flow behavior, segregation potential, and mechanical application efficiency. The key findings of the study are summarized below:

- The percentile-based granule size indices (d5, d16, d84, and d90) varied considerably among the ten urea manufacturers, indicating significant differences in granule size across commercial brands.

- d5 values ranged from 0.394 to 0.861 mm, with the lowest value for Sample III and the highest for Sample IX. Similarly, d16 values ranged from 0.650 to 0.943 mm, with Samples III and IV showing the minimum and maximum values, respectively.

- d84 values ranged from 1.311 to 1.484 mm, indicating variability in the coarser granule fraction. Sample III exhibited the lowest d84 and Sample IX the highest. d90 values ranged from 1.359 to 1.565 mm, with clear variation across samples.

- The coefficients of variation for all percentile diameters were generally below 5%.

- One-way ANOVA revealed statistically significant differences across all percentile diameters studied, and Tukey’s post-hoc comparisons confirmed that the majority of manufacturer pairs differed significantly for each d-value.

- The granule size indices presented provide foundational data useful for calculating uniformity indices, enabling quantitative assessment of fertilizer distribution quality in field application.

- The results can also be utilized in particle simulation models of urea fertilizer, supporting virtual testing of flow behavior, metering accuracy, and machine design optimization.

Disclaimer (Artificial intelligence)

Author(s) hereby declare that generative AI technologies such as Large Language Models, etc. have been used for improving the grammar, language clarity, and overall readability of the manuscript. Details of the AI usage are given below:

1. ChatGPT (version 5.2)

References

- Allaire, S. E., & Parent, L. E. (2004). Physical Properties of Granular Organic-based Fertilisers, Part 2: Dynamic Properties Related to Water. Biosystems Engineering, 87(2), 225–236. https://doi.org/10.1016/j.biosystemseng.2003.09.007

- Amiri, H., Kianmehr, M. H., & Arabhosseini, A. (2019). Effect of particle size, die rotary speed and amount of urea on physical properties of the produced pellet. International Journal of Environmental Science and Technology, 16(4). https://doi.org/10.1007/s13762-017-1627-1

- Anonymous. (2024). Annual Report 2023-24, Department of Fertilizers, Ministry of Chemicals & Fertilizers, Government of India, New Delhi.

- Bhatti, M. E. (1992). Physical properties comparative study of urea of different companies in Pakistan. Fertilizer Research, 32, 13–17. https://doi.org/10.1007/BF01054389

- Cousins, J. D. M., Roberge, M. J., & Tabil, L. G. (2021). Measuring the physical properties of granular fertilizer in relation to flow. 5th International Conference of the International Commission of Agricultural and Biosystems Engineering (CIGR), 1–10.

- Fulton, J., & Port, K. (2016). Physical Properties of Granular Fertilizers and Impact on Spreading. https://ohioline.osu.edu/factsheet/fabe-5501

- Gavrilović, M., Dimitrijević, A., Radojičin, M., Mileusnić, Z., & Miodragović, R. (2018). Effects of the application system on the physical and mechanical properties of mineral fertilizers. Journal on Processing and Energy in Agriculture, 22(4), 180–183. https://doi.org/10.5937/jpea1804180G

- Glibert, P. M., Harrison, J., Heil, C., & Seitzinger, S. (2006). Escalating worldwide use of urea - A global change contributing to coastal eutrophication. Biogeochemistry, 77, 441–463. https://doi.org/10.1007/s10533-005-3070-5

- ISO 8397:1988. (1988). Solid ferttilizers and soil conditioners - Test sieving. https://standards.iteh.ai/catalog/standards/sist/2979df18-b1f1-4783-b91f-

- Kumar, V., Rajan, P., Deshmukh, M. M., Gupta, C., Thakare, S. K., Thakare, S. H., Gajakos, A. V., & Kanade, S. A. (2025). Comparative study of particle size distribution in commercial urea fertilizers from India. International Journal of Research in Agronomy, 8(7), 10–13. https://doi.org/https://www.doi.org/10.33545/2618060X.2025.v8.i7Sa.3189

- Miserque, O., & Pirard, E. (2004). Segregation of the bulk blend fertilizers. Chemometrics and Intelligent Laboratory Systems, 74(1), 215–224. https://doi.org/10.1016/j.chemolab.2004.03.017

- Perfect, E., Xu, Q., & Terry, D. L. (1998). Improved parameterization of fertilizer particle size distribution. Journal of AOAC International, 81(5), 935–942. https://academic.oup.com/jaoac/article/81/5/935/5684045

- Rahmanian, N., Naderi, S., Supuk, E., Abbas, R., & Hassanpour, A. (2015). Urea finishing process: Prilling versus granulation. Procedia Engineering, 102, 174–181. https://doi.org/10.1016/j.proeng.2015.01.122

- Rutland, D. W. (1986). Manual for determining physical properties of fertilizer.

- Shamsudin, I. S., Anuar, M. S., Yusof, Y. A., Mohd, A. H., & Tahir, S. M. (2014). Effect of Particle Size on Direct Compaction of Urea Fertilizer. Particulate Science and Technology: An International Journal, 32(6), 544–553. https://doi.org/10.1080/02726351.2014.930942

- Simsek, H. M., & Guliyev, R. (2021). The investigation of physical properties of composite fertilizer including boron micro element. Sakarya University Journal of Science, 25(5), 1245–1252. https://doi.org/10.16984/saufenbilder.853343

- Virk, S. S., Mullenix, D. K., Sharda, A., Hall, J. B., Wood, C. W., Fasina, O. O., McDonald, T. P., Pate, G. L., & Fulton, J. P. (2013). Case study: Distribution uniformity of a blended fertilizer applied using a variable-rate spinner-disc spreader. Applied Engineering in Agriculture, 29(5), 627–636. https://doi.org/10.13031/aea.29.9774

- M. K. Gamit, V. G. Bavalgave, V. N. Shiyal & R. P. Vaja. (2023). Effect of Different Rates and Times of Nitrogen Application on Growth, Yield Attributes and Yield of Sweet Corn (Zea mays L. saccharata) Under South Gujarat Condition. International Journal of Plant & Soil Science, 35(19), 937–945. https://doi.org/10.9734/ijpss/2023/v35i193628