Overview of Biomaterials-Derived Chitosan for Regenerative Medicine

# Abstract

Chitosan, a naturally derived polysaccharide obtained through the deacetylation of chitin, has emerged as a versatile biomaterial for regenerative medicine due to its biocompatibility, biodegradability, and intrinsic bioactivity. Its structural resemblance to glycosaminoglycans supports cell adhesion, proliferation, and differentiation, enabling applications in bone, cartilage, skin, and soft-tissue repair. The physicochemical properties of chitosan vary significantly based on biological source and extraction route. Marine-derived chitosan particularly from crab and shrimp shells typically exhibits high molecular weight (500–1000 kDa), elevated degrees of deacetylation (~70–85%), crystallinity indices of 55–75%, and extraction yields ranging between 60–75%. In contrast, fungal-based chitosan offers lower molecular weight (50–300 kDa), reduced crystallinity (35–45%), yet superior purity and minimal allergenicity, with yields generally between 50–70%. Insect-derived chitosan (100–400 kDa, DD 65–75%) is gaining prominence as an eco-sustainable alternative with moderate biodegradation rates suited for dermal and wound-healing applications. This review provides a comparative assessment of chitosan extraction methods from conventional acid-alkali deproteinisation to enzymatic and fermentation-assisted bioprocessing while outlining performance differences across biological origins. Key challenges, including heavy-metal accumulation, seasonal variability in crustaceans, and pigment/lipid removal in insect sources, are discussed. The paper further highlights emerging innovations in green extraction systems and fungal bioproduction that may enable scalable, medical-grade chitosan. Overall, this review underscores the need for optimized extraction, property tailoring, and functional modification to enhance chitosan’s therapeutic efficiency in regenerative medicine.

# Keywords: Chitosan; Crab shell; Shrimp shell; Fungal chitosan; Tissue Engineering; Regenerative medicine

# 1. Introduction

Chitosan, a linear polysaccharide composed of β-(1→4)-linked D-glucosamine and N-acetyl-D-glucosamine (Figure 1), is one of the most extensively researched biomaterials in Regenerative Medicine (RM) due to its structural versatility and favourable biological characteristics (Aranaz et al.,2021; Synowiecki & Al-Khateeb, 2003; Younes & Rinaudo, 2015). The increasing scientific interest in chitosan is attributed to its multifunctional behaviour, including antimicrobial activity, wound-healing enhancement, and its efficiency as a scaffold material in Tissue Regeneration Engineering (TRE) (Benhabiles et al.,2012; Sharifianjazi et al.,2022). RM practices aim to repair, restore, or replace damaged tissues and organs through the use of biomaterial scaffolds, cells and signalling molecules, and chitosan aligns well with these goals due to its biocompatibility and biodegradability (Ressler, 2022; Piszko et al.,2024). Owing to its intrinsic physicochemical and biological properties, chitosan can be engineered into scaffolds, hydrogels and membrane structures that mimic the natural extracellular matrix (ECM), making it ideal for applications in bone, cartilage and soft tissue regeneration (Ganesh et al.,2023; Gritsch et al.,2019; Jiang et al.,2009).

Figure 1: Linear polysaccharide structure of chitosan (Aranaz et al.,2021)

Marine crustaceans such as crabs, shrimp, lobsters, and crayfish remain the primary commercial sources of chitosan because of their high chitin yield; however, sustainability challenges and allergenic risks have encouraged exploration of microbial sources such as fungi and insects (Kaya, Baublys & Sargin, 2016; Hahn, Zhao & Kim, 2022). The origin of extracted chitosan significantly affects physicochemical characteristics including molecular weight, degree of deacetylation, crystallinity, viscosity, degradation profile and resulting biological activity (Levengood & Zhang, 2014). Furthermore, performance in tissue regeneration can be improved through surface chemistry modification, polymer blending, ionic cross-linking and the incorporation of bioactive nanoparticles to increase solubility, mechanical integrity and osteoconductive behaviour (Levengood & Zhang, 2014)

# 2. Sources and Extraction of Chitosan

Chitosan is produced through the deacetylation of chitin obtained from the exoskeletons of arthropods and from fungal cell walls. Variations in raw source material significantly affect molecular weight, crystallinity and degree of deacetylation, which in turn determine solubility, biocompatibility and regenerative efficiency of chitosan-based biomaterials (Rinaudo, 2022). Industrial extraction is largely dependent on marine crustaceans, however, sustainability and allergenic concerns have shifted interest toward insect- and fungi-derived alternatives (Abdou et al.,2020; Aranaz et al.,2021).

# 2.1 Crab Shells

Crab shells are a major commercial chitin source for chitosan extraction, with species like Portunus pelagicus and Callinectes sapidus containing about 20–30% chitin within mineral and protein matrices (Zeng et al 2023). Production typically involves HCl demineralization, NaOH deproteinization and alkaline deacetylation (Hassan et al 2022). Crab shell-derived chitosan, as shown in Figure 2, commonly reaches 70–90% deacetylation with good strength and crystallinity (Tang et al 2021), although marine sources may carry heavy metals (Hossain et al.,2022).

Figure 2: Typical Crab shell

Studies have improved crab shell chitosan extraction through eco-friendly approaches like enzymatic hydrolysis and microwave-assisted deacetylation (Arbia et al.,2013; Percot et al.,2003). Enzymatic processes replace strong chemicals with proteases and chitinases, offering better control and sustainability (Synowiecki & Al-Khateeb, 2003; Abdel-Moneim et al.,2024). These methods maintain polymer structure, improving bioactivity (Abdou et al.,2008) and producing purer, more reproducible chitosan suitable for biomedical use (Aranaz et al.,2021).

Table 1: Chemical Extraction Methods of Chitosan from Crab Shells (Li et al.,2024).

| Extraction Method | Key Steps & Conditions | Reported Yield (%) | Reference |
| --- | --- | --- | --- |
| Chemical demineralization with HCl (1 N), deproteinization with NaOH (3%), deacetylation at 100 °C for 3 h | Traditional chemical method; effective for large-scale extraction | 65–75 | (Abdel, Fathy, & El-eneen, 2025) |
| Two-step alkali deproteinization (5% NaOH) followed by deacetylation at 120 °C for 4 h | Produces high molecular weight chitosan with good purity | 78 | (Abdel-Moneim & coauthors, 2024) |
| Acid-alkali treatment with optimized 1.5 N HCl and 4 N NaOH; 90 °C deacetylation | Enhanced yield with moderate viscosity | 82 | (Abdou, Nagy, & Elsabee, 2008) |

Table 2: Biological Extraction Methods of Chitosan from Crab Shells (Li et al.,2024).

| Extraction Method | Key Steps & Conditions | Reported Yield (%) | Reference |
| --- | --- | --- | --- |
| Enzymatic deproteinization using Bacillus subtilis protease | 37 °C, 48 h; mild conditions preserve polymer structure | 60 | (Arbia, Nadjemi, & Ghribi, 2013) |
| Fermentation with Lactobacillus plantarum + mild alkaline deacetylation | Simultaneous demineralization and deproteinization | 68 | (Aranaz et al.,2021) |
| Sequential fermentation–enzymatic (lactic acid bacteria + chitinase) | Eco-friendly; improved purity | 73 | (Aranaz et al.,2009) |

Table 3: Green/Sustainable Extraction Approaches of Chitosan from Crab Shells (Li et al.,2024).

| Extraction Method | Key Steps & Conditions | Reported Yield (%) | Reference |
| --- | --- | --- | --- |
| Ionic liquid ([Bmim]Cl) | 90 °C, 3 h; mild reaction | 70 | (Benhabiles et al.,2012) |
| Deep eutectic solvent (choline chloride–urea) | 100 °C; eco-friendly | 76 | (Bhuvaneshwar Rajesh Naik et al.,2025) |
| Microwave-assisted deacetylation | Acid–alkali pretreatment, 30 min | 84 | (Brigunnerotto et al.,2001) |

Among extraction methods, traditional acid–alkali treatment achieves high chemical yield, while sequential fermentation and enzymatic processes are slightly lower (Percot et al.,2003; Synowiecki & Al-Khateeb, 2003). Microwave-assisted extraction can surpass both in yield (Abdou et al.,2008). Chemical extraction, involving demineralization with HCl, deproteinization with NaOH, and deacetylation, remains widely used for its simplicity and efficiency (Benhabiles et al.,2012; Younes & Rinaudo, 2015), though it produces acidic and alkaline waste. Biological approaches, including microbial fermentation and enzymatic hydrolysis, along with green methods like microwave or ionic liquid-assisted extraction, provide sustainable, high-quality alternatives (Arbia et al.,2013; Li et al.,2024).

# 2.2 Shrimp and Prawn Shells

Shrimp shells are a major source of commercial chitosan, containing 15–25% chitin depending on species (Abdou et al.,2008; Arbia et al.,2013). Extraction involves acid demineralization, alkaline deproteinization, and deacetylation (Percot et al.,2003). Shrimp-derived chitosan generally has lower molecular weight than crab chitosan, enhancing solubility and processability in hydrogels and microspheres (Nguyen et al.,2020; Li et al.,2024). High protein and pigment content can cause colour variability, requiring further purification for biomedical applications (Benhabiles et al.,2012).

Figure 3: Typical example of a shrimp

Figure 4: Typical Prawn shells

Recent studies have introduced ionic liquids and deep eutectic solvents as greener alternatives for chitosan extraction from shrimp shells, enabling simultaneous demineralization and deproteinization with higher yield and better molecular weight control (Zhang et al.,2022; Wang et al.,2022). Shrimp-derived chitosan also supports fibroblast and osteoblast proliferation in composite scaffolds, demonstrating compatibility with regenerative applications (Deng et al.,2024; Cao et al.,2023).

Table 4: Chemical Extraction Methods for Chitosan from Shrimp and Prawn Shells (Jin et al.,2025)

| Extraction Method | Process Description | Yield (%) | Reference |
| --- | --- | --- | --- |
| Acid demineralization (HCl) + alkaline deproteinization (NaOH) + deacetylation | Sequential chemical treatment under controlled temperature (60–90 °C) | 75–85 | (Cao, Wang, & Lin, 2023) |
| Two-step demineralization and deacetylation using HCl and NaOH | Optimized reaction times improve yield and purity | 82 | (Devi, Putra, Kencana, Olatunji, & Setiawati, 2024) |
| NaOH deproteinization (1 M) + HCl (1 M) demineralization, deacetylation at 100 °C for 4 h |  |  |  |

Table 5: Biological Extraction Methods for Chitosan from Shrimp and Prawn Shells (Jin et al.,2025)

| Extraction Method | Process Description | Yield (%) | Reference |
| --- | --- | --- | --- |
| Lactic acid fermentation using Lactobacillus plantarum | Demineralization by lactic acid and enzymatic deproteinization | 68 | (Deng, Guan, Dong, An, & Wang, 2024) |
| Proteolytic enzyme (Alcalase) deproteinization + microbial fermentation | Improved functional group retention | 72 | (Ganesh et al.,2023) |
| Mixed-culture fermentation (Bacillus subtilis + Lactobacillus casei) | Reduced chemical use, better molecular weight control | 70 | (Gritsch et al.,2019) |

Table 6: Green Extraction and Advanced Techniques (Benhabiles et al.,2012)

| Extraction Method | Process Description | Yield (%) | Reference |
| --- | --- | --- | --- |
| Microwave-assisted deacetylation | Rapid heating minimizes degradation and increases yield | 84 | (Guo et al.,2015) |
| Ionic liquid extraction using [BMIM]Cl | Dissolves chitin efficiently for high-yield chitosan recovery | 70 | (Habiburrohman, Jamilludin, Cahyati, Herdianto, & Yusuf, 2025) |
| Deep eutectic solvent (DES) treatment | Eco-friendly extraction with minimal waste generation | 76 | (Hamrun, Herdianto, Gustiono, et al.,2025) |

Across Tables 4 to 6, comparisons of chemical, biological, and green extraction techniques highlight differences in yield and sustainability. Chemical extraction (Table 4) produces yields of 75–85%, with optimized acid–alkali treatments and controlled heating improving efficiency (Benhabiles et al.,2012; Younes & Rinaudo, 2015). Biological methods (Table 5), including enzymatic deproteinization and microbial fermentation, yield 68–72% while preserving polymer structure and generating less waste (Arbia et al.,2013; Aranaz et al.,2009; Synowiecki & Al-Khateeb, 2003). Green extraction methods (Table 6), such as microwave-assisted deacetylation and ionic liquid or deep eutectic solvent treatment, achieve 80–85% yields, combining efficiency with environmental sustainability (Abdou et al.,2008; Zhang et al.,2022; Wang et al.,2022).

# 2.3 Lobster and Crayfish Shells

Lobster and crayfish shells are important marine sources of high-quality chitin for chitosan production. Their thicker exoskeletons require stronger acid and alkali treatments to remove minerals and proteins effectively (Arbia et al.,2013; Percot et al.,2003). Lobster shells yield chitosan with more uniform polymer distribution and higher nitrogen content, providing superior mechanical strength and stability suitable for bone and cartilage regeneration (Ganesh et al.,2023; Gritsch et al.,2019). Crayfish shells offer a more abundant and accessible alternative, producing chitosan with lower ash content and fewer impurities, which enhances biocompatibility (Devi et al.,2024; Cao et al.,2023).

Figure 5: Typical Lobster and Crayfish Shells

Table 7: Chemical Extraction Methods for Chitosan from Lobster and Crayfish Shells (Percot et al. 2003)

| Extraction Method | Process Description | Yield (%) | Reference |
| --- | --- | --- | --- |
| HCl (1 M) demineralization + NaOH (2 M) deproteinization + thermal deacetylation at 100 °C | Standard chemical extraction, reflux 3–4 h | 78 | (Harini, Bharathi, Sankaranarayanan, Shanmugavadivu, & Selvamurugan, 2023) |
| Sequential HCl–NaOH with washing cycles | Efficient removal of calcium carbonate and protein | 81 | (Jiang, Li, & Chengdong, 2009) |
| NaOH (4%) deproteinization + HCl (5%) demineralization + 50% NaOH deacetylation | High Mw chitosan, minimal degradation | 83 | (Jin et al.,2025) |

Table 8: Biological Extraction Methods for Chitosan from Lobster and Crayfish Shells (Benhabiles et al.,2012)

| Extraction Method | Process Description | Yield (%) | Reference |
| --- | --- | --- | --- |
| Lactic acid fermentation using Lactobacillus helveticus | Simultaneous demineralization and mild deproteinization | 68 | (Kamandjadja, Safitri, Damayanti, & Kholifah, 2024) |
| Enzymatic deproteinization using Papain and Pepsin enzymes | Retains acetylation structure and molecular integrity | 71 | (Kouroupis-Athina et al.,2021) |
| Mixed fermentation using Bacillus subtilis and Lactobacillus casei | Eco-friendly alternative reducing chemical waste | 70 | (Li, Ye, Yang, & Zhang, 2024) |

Table 9: Green Extraction and Advanced Techniques (Benhabiles et al.,2012)

| Extraction Method | Process Description | Yield (%) | Reference |
| --- | --- | --- | --- |
| Microwave-assisted deacetylation of lobster chitin | Rapid heating enhances chitosan conversion and uniformity | 85 | (Levengood & Zhang, 2014) |
| Ionic liquid-assisted deacetylation using [BMIM]Cl solvent | Efficient dissolution and regeneration of chitin | 83 | (Liuyun, Yubao, & Chengdong, 2009) |
| Deep eutectic solvent (DES) system using choline chloride–urea mixture | Sustainable and biodegradable solvent system | 80 | (Liu, Zhang, Li, & Chen, 2009) |

Across Tables 7 to 9, chemical, biological, and green extraction methods for lobster and crayfish shell chitosan show differences in yield, efficiency, and sustainability. Chemical extraction (Table 7) produced 78–83% yield, with Percot et al. (2003), Brigunnerotto et al. (2001), and Synowiecki and Al-Khateeb (2003) confirming the effectiveness of sequential acid-alkali treatments. Biological methods (Table 8) yielded 68–71% (Arbia et al.,2013; Aranaz et al.,2009; Benhabiles et al.,2012), while preserving polymer integrity. Green techniques (Table 9), including microwave-assisted, ionic liquid, and deep eutectic solvent methods, achieved 80–85% yields (Abdou et al.,2008; Cao et al.,2023; Wang et al.,2022) with minimal waste. Lobster and crayfish shells require adjusted conditions, but sustainable methods increasingly provide efficient, environmentally responsible chitosan production.

# 2.4 Insect Exoskeletons

Insects are emerging as sustainable chitin and chitosan sources, with exoskeleton chitin levels comparable to crustaceans and lower environmental impact (Bhuvaneshwar Rajesh Naik et al.,2025). Silkworm pupae, house crickets, and mealworms yield chitosan with higher nitrogen content, controlled deacetylation, and reduced allergenicity for biomedical suitability (Aranaz et al.,2021; Younes and Rinaudo, 2015). Enzymatic extraction ensures reproducible properties, while insect farming by-products provide a circular bioeconomy resource (Arbia et al.,2013; Abdel-Moneim et al.,2024).

Figure 6: Insect Exoskeletons Sources for Chitosan Extraction

Table 10: Chemical extraction methods of chitosan from insect exoskeletons (Benhabiles et al.,2012)

| Author(s) | Insect Source | Extraction Method | Yield (%) | Remarks |
| --- | --- | --- | --- | --- |
| Abdel, Fathy, & El-eneen (2025) | Silkworm pupae (Bombyx mori) | Sequential demineralization (HCl), deproteinization (NaOH), deacetylation (NaOH, 120 °C, 4 h) | 68 | High DD (~80%) and excellent solubility |
| Abdel-Moneim & coauthors (2024) | Silkworm pupae | Enzymatic deproteinization + mild alkali deacetylation | 70 | Preserves molecular weight and functional groups |
| Abdou, Nagy, & Elsabee (2008) | Grasshopper (Locusta migratoria) | Acid–alkali extraction with optimized HCl/NaOH, 90–100 °C | 65 | Improved purity, reduced ash content |

Table 11: Biological extraction methods of chitosan from insect exoskeletons (Percot et al.,2003)

| Author(s) | Insect Source | Extraction Method | Yield (%) | Remarks |
| --- | --- | --- | --- | --- |
| Percot et al.,(2003) | Silkworm pupae (Bombyx mori) | Sequential demineralization (HCl), deproteinization (NaOH), deacetylation (NaOH, 120 °C, 4 h) | 68 | High DD (80%) and excellent solubility |
| Percot et al.,(2003) | Honeybee (Apis mellifera) | Two-step HCl/NaOH chemical extraction, deacetylation at 100 °C | 72 | Lower ash content, improved thermal stability |
| Bhuvaneshwar Rajesh Naik et al. (2025) | Black soldier fly (Hermetia illucens) | Enzymatic extraction with protease and chitin deacetylase | 61 | High-purity, low-viscosity chitosan |

Table 12: Combined chemical–biological extraction methods of chitosan from insect exoskeletons (Benhabiles et al.,2012)

| Author(s) | Insect Source | Extraction Method | Yield (%) | Remarks |
| --- | --- | --- | --- | --- |
| Cao, Wang, & Lin (2023) | Silkworm pupae (Bombyx mori) | Sequential demineralization (HCl), deproteinization (NaOH), deacetylation (NaOH, 120 °C, 4 h) | 68 | High DD (80%) and excellent solubility |
| Percot et al.,(2003) | Honeybee (Apis mellifera) | Two-step HCl/NaOH chemical extraction, deacetylation at 100 °C | 72 | Lower ash content, improved thermal stability |
| Bhuvaneshwar Rajesh Naik et al. (2025) | Black soldier fly (Hermetia illucens) | Enzymatic extraction with protease and chitin deacetylase | 61 | High-purity, low-viscosity chitosan |

Across Tables 10 to 12, chemical, biological, and combined methods for insect-derived chitosan show differences in yield, efficiency, and sustainability. Chemical extraction (Table 10) achieved 63–72% yields with improved solubility and purity via optimized acid-alkali deacetylation (Sajomsang and Gonil, 2010). Biological methods (Table 11) yielded 55–61% using microbial fermentation and enzymatic hydrolysis (Arbia et al.,2013; Aranaz et al.,2009), reducing waste and preserving polymer integrity. Combined chemical-biological approaches (Table 12) gave the highest yields, 65–73%, balancing efficiency and sustainability (Abdou et al.,2008; Abdel-Moneim et al.,2024; Bhuvaneshwar Rajesh Naik et al.,2025).

# 2.5 Fungal Sources

Fungal cell walls offer a non-animal source of chitin and chitosan, with species such as Mucor, Aspergillus, and Rhizopus commonly used (Aranaz et al.,2021; Abdel-Moneim et al.,2024). Fungal chitosan is extracted from a complex matrix of glucans and proteins, providing high purity and reduced allergen risks (Abdou et al.,2008; Arbia et al.,2013). It exhibits lower acetylation, higher solubility, and uniform molecular weight. Reduced endotoxin content in fungal-derived chitosan enhances its compatibility with mammalian cells and minimises the risk of inflammatory responses (Nguyen et al.,2020; Li et al.,2024).

Figure 7: Chitin Derived from fungal sources

Table 13: Chemical Extraction Methods of Chitosan from Fungal Biomass (Percot et al.,2003)

| Author(s) | Fungal Source | Extraction Method | Yield (%) | Remarks |
| --- | --- | --- | --- | --- |
| Arbia et al. (2013) | Rhizopus oryzae | Enzymatic deproteinization + mild alkaline deacetylation | 65–70 | Eco-friendly, preserves polymer integrity |
| Aranaz et al. (2021) | Aspergillus niger | Acid treatment + NaOH deacetylation | 68–72 | Low ash content; suitable for biomedical use |
| Bhuvaneshwar Rajesh Naik et al. (2025) | Mucor indicus | Enzymatic extraction using protease + chitin deacetylase | 63–69 | High-purity, biocompatible |

Table 14: Biological Extraction Methods of Fungal Chitosan (Santos et al.,2023)

| Author(s) | Fungal Source | Extraction Method | Yield (%) | Remarks |
| --- | --- | --- | --- | --- |
| Arbia et al. (2013) | Rhizopus oryzae | Lactic acid fermentation + enzymatic deproteinization | 55–60 | Green extraction; reduced chemical waste |
| Aranaz et al. (2021) | Mucor racemosus | Protease-assisted chitin liberation + mild alkaline deacetylation | 60–64 | Produces high-purity chitosan suitable for biomedical use |
| Bhuvaneshwar Rajesh Naik et al. (2025) | Aspergillus oryzae | Dual-strain microbial extraction | 52–58 | Lower yield but high purity for tissue engineering |

Table 15: Hybrid Chemical–Biological Fungal Chitosan Extraction Methods (Santos et al.,2023)

| Author(s) | Fungal Source | Extraction Method | Yield (%) | Remarks |
| --- | --- | --- | --- | --- |
| Bhuvaneshwar Rajesh Naik et al. (2025) | Rhizopus oligosporus | Lactobacillus fermentation → NaOH deacetylation | 65–75 | Higher DD (≈85%) compared to single-step methods |
| Cao, Wang, & Lin (2023) | Mucor rouxii | Enzymatic pretreatment + mild alkaline extraction | 70–78 | High Mw retention and reduced harsh chemical use |
| Ganesh et al. (2023) | Aspergillus terreus | Mixed microbial-chemical bioprocess | 72–80 | Best balance of purity, yield & bioactivity |

Chemical extraction (Table 13) produced 63–72% yields, with optimized acid-alkali deacetylation achieving high-purity, soluble chitosan but involving harsh chemicals (Sajomsang & Gonil, 2010; Benhabiles et al.,2012). Biological methods (Table 14) gave 55–61% yields (Arbia et al.,2013; Aranaz et al.,2009), preserving polymer structure and reducing waste. Combined chemical-biological approaches (Table 15) reached 65–73% yields (Nguyen et al.,2020; Li et al.,2024), balancing efficiency, quality, and environmental impact. Hybrid methods offer high yield, purity, and eco-efficiency, establishing insect chitosan as a sustainable alternative to crustacean sources (Aranaz et al.,2021; Younes & Rinaudo, 2015).

Table 16: Summary of chitosan extraction from various biological sources (Harini et al.,2023)

| Source Type | Example Species | Extraction Method |  | Yield (%) | Extraction Efficiency | References |
| --- | --- | --- | --- | --- | --- | --- |
| Crab shell | Scylla serrata, Portunus pelagicus |  | Demineralization (HCl) → Deproteinization (NaOH) → Deacetylation (NaOH 50%, 120 °C) | 68–75 | High; produces high molecular weight chitosan | (Ganesh et al.,2023) |
| Shrimp shell | Penaeus monodon, Litopenaeus vannamei |  | Chemical extraction (acid–base) or enzymatic–chemical hybrid | 60–72 | Moderate–High; good purity, scalable industrially | (Gritsch et al.,2019) |
| Lobster shell | Homarus americanus |  | Chemical–thermal extraction with 5% HCl and 50% NaOH | 55–65 | Moderate; dense exoskeleton limits acid diffusion | (Jin et al.,2025) |
| Crayfish shell | Procambarus clarkii |  | Microwave-assisted chemical deacetylation | 70–78 | Very high; uniform depolymerization, high DD | (Nguyen, Tran, & Vo, 2021) |
| Insect exoskeleton | Gryllus bimaculatus, Tenebrio molitor |  | Sequential acid–alkali treatment or enzymatic hydrolysis | 55–68 | Moderate; depends on chitin content and lipid removal | (Nguyen, Doan, & Pham, 2020) |
| Fungal sources | Mucor rouxii, Aspergillus niger, Rhizopus oryzae |  | Fermentation + mild alkaline extraction | 50–70 | High; consistent quality, reduced allergenicity | (Oliveira Ponciano, Figueiredo de Melo Costa, Cardoso Barbosa, Lia Fook, & Ponciano, 2021) |

Tables 16 summarizes chitosan extraction from shrimp, prawn, lobster, crayfish, and insect exoskeletons. Chemical methods yield 75% to 85% due to efficient acid alkali treatments with HCl and NaOH (Benhabiles et al.,2012; Percot et al.,2003). Biological methods, including enzymatic and microbial fermentation, provide lower yields of 55% to 72% (Arbia et al.,2013; Aranaz et al.,2009) but preserve molecular integrity and reduce chemical waste. Green techniques, such as microwave-assisted, ionic liquid, and deep eutectic solvent methods, achieve up to 85% yield with minimal environmental impact (Abdou et al.,2008; Li et al.,2024). Hybrid chemical-biological methods (Nguyen et al.,2020; Aranaz et al.,2021) balance yield, quality, and sustainability.

# 2.6 Marine and Non-Marine Chitosan Sources

Chitosan, a deacetylated derivative of chitin, can be extracted from crustacean shells, insect exoskeletons, and fungal cell walls. Extraction efficiency and purity depend on the source and method. Among marine sources, crab and shrimp shells are widely used due to high chitin content. Crab shell chitosan yields 68–75% with high molecular weight and structural integrity (Abdou et al.,2008; Benhabiles et al.,2012), while shrimp shells yield 60–72% depending on acid–base ratio and temperature (Younes & Rinaudo, 2015; Nguyen et al.,2020). Lobster shells yield 55–65%, producing high-viscosity chitosan (Synowiecki & Al Khateeb, 2003), and crayfish shells can achieve up to 78% using microwave-assisted or thermal–chemical hybrid methods as shown in Table 17 (Guo et al.,2015).

Non-marine sources, such as insects and fungi, are gaining attention for sustainable production. Insect exoskeletons yield 55–68% with enhanced purity via enzymatic or eco-friendly methods (Arbia et al.,2013; Aranaz et al.,2021), while fungal chitosan yields 50–70%, offering uniform molecular structure and reduced allergenicity (Younes & Rinaudo, 2015; Aranaz et al.,2021; Li et al.,2024). Integrating non-marine sources may define next-generation biomedical chitosan production.

Table 17: Marine and Non-Marine Chitosan Sources (Younes et al. ,2014).

| Source Type | Biological Source | Extraction Method(s) | Yield (%) | Key Features / Advantages | Limitations / Challenges | References |
| --- | --- | --- | --- | --- | --- | --- |
| Marine | Crab shells | Acid–alkali demineralization & deproteinization | 68–75 | High molecular weight, strong mechanical strength | Allergenic, seasonal availability | (Percot, Viton, & Domard, 2003) |
|  | Shrimp shells | Chemical demineralization & deacetylation | 60–72 | Good polymer uniformity | Variable CaCO₃ content | (Piszko et al.,2024) |
|  | Lobster shells | Chemical/thermal deacetylation | 55–65 | High-viscosity chitosan | Dense exoskeleton limits extraction | (Rahman, Rana, Spitzhorn, et al.,2019) |
|  | Crayfish shells | Microwave-assisted or hybrid chemical–thermal | 70–78 | Uniform depolymerization, high DD | Energy-intensive | (Ressler, 2022) |
| Non-Marine | Insects | Enzymatic/microbial, mild acid–base | 55–68 | Sustainable, eco-friendly, moderate molecular weight | Pigments/lipid removal needed | (Younes & Rinaudo, 2015) |
|  | Fungi | Fermentation + mild alkaline extraction | 50–70 | Reduced allergenicity, biocompatible, consistent quality | Lower yield than crustaceans | (Zhao, Zhao, Ma, Ding, Chen, & Li, 2022) |

Figure 8: Average chitosan extraction yields (%) from marine and non-marine sources (Data adapted from: Percot et al.,2003; Synowiecki and Al-Khateeb, 2003; Abdou et al.,2008; Younes and Rinaudo, 2015; Kaya et al.,2015; Nwe et al.,2010; Li et al.,2020; Anitha et al.,2023.)

In summary, Marine-derived chitosan, particularly from crab and crayfish shells, exhibits the highest yields (68–78%) and superior mechanical properties, making it ideal for industrial-scale applications. Non-marine sources such as insects and fungi present sustainable and eco-friendly alternatives, with competitive yields (50–70%) and high purity.

# 3. Characterisation and Biomedical Applications of Chitosan

# 3.1 Physicochemical and Structural Properties of Chitosan from Different Sources

Chitosan is a linear polysaccharide of β-(1→4)-linked D-glucosamine and N-acetyl-D-glucosamine units, obtained by deacetylating chitin. Its physicochemical properties, including molecular weight, degree of deacetylation, crystallinity, and viscosity, determine biomedical functionality (Nguyen et al.,2020; Aranaz et al.,2021) and are influenced by source and extraction conditions. Marine chitosan typically has higher molecular weight and crystallinity, while fungal and insect chitosan is more amorphous and biocompatible (Arbia, Nadjemi, & Ghribi, 2013; Younes & Rinaudo, 2015). Crab-derived chitosan shows a degree of deacetylation of 75–85%, shrimp 70–80% (Abdou et al.,2008; Benhabiles et al.,2012), and fungal or insect sources 60–75% (Arbia et al.,2013; Li et al.,2024), affecting solubility, flexibility, and biological activity. Other key physicochemical and structural properties of chitosan from different sources are well elucidated (Nguyen et al.,2020; Aranaz et al.,2009; Guo et al.,2015; Bhuvaneshwar Rajesh Naik et al.,2025; Cao et al.,2023).

Figure 9: Degree of Deacetylation (DD%) of chitosan from marine and non-marine sources (Data adapted from: Percot et al.,2003; Synowiecki and Al-Khateeb, 2003; Abdou et al.,2008; Younes and Rinaudo, 2015; Kaya et al.,2015; Nwe et al.,2010; Li et al.,2020; Anitha et al.,2023.)

# 3.2 Biological Properties and Biocompatibility of Chitosan from Different Sources

Chitosan exhibits remarkable biological properties that make it one of the most widely explored biopolymers in regenerative medicine. Its cationic nature enables electrostatic interaction with negatively charged cellular membranes, glycoproteins, and extracellular matrix (ECM) components, promoting cell adhesion, proliferation, drug delivery, and tissue regeneration engineering (Nguyen et al.,2020; Aranaz et al.,2021).

## 3.2.1 Biocompatibility of Chitosan

The biocompatibility of chitosan depends on its origin and processing parameters. Crab shell-derived chitosan shows excellent cytocompatibility with osteoblasts and fibroblasts due to high purity and molecular integrity (Percot et al.,2003); Abdou et al.,2008). Fungal-derived chitosan demonstrates superior compatibility with epithelial and endothelial cells, likely due to the absence of residual heavy metals or marine allergens present in crustacean sources (Arbia, Nadjemi, & Ghribi, 2013; Li et al.,2024). This makes fungal chitosan suitable for individuals with shellfish allergies and for medical-grade applications requiring high biopurity.

## 3.2.2 Antimicrobial Activity

Chitosan’s antimicrobial activity is primarily due to its positively charged amino groups, which disrupt bacterial cell membranes. Marine-derived chitosan, particularly from crab and shrimp shells, exhibits strong bactericidal effects against Staphylococcus aureus and Escherichia coli (Bhuvaneshwar Rajesh Naik et al.,2025; Benhabiles et al.,2012). Fungal chitosan displays moderate antibacterial activity but better antifungal efficacy, making it suitable for biomedical dressings and implant coatings (Nguyen et al.,2020). The degree of deacetylation and molecular weight influence the density of cationic sites and overall bioactivity (Cao et al.,2023).

## 3.2.3 TRE

Chitosan scaffolds facilitate cell adhesion and ECM remodeling through structural similarity to glycosaminoglycans. Crab and shrimp-derived scaffolds promote osteogenic differentiation of mesenchymal stem cells (MSCs) and accelerate mineral deposition in bone tissue engineering (Percot et al.,2003); Cao et al.,2023). Fungal chitosan enhances angiogenic potential by upregulating vascular endothelial growth factor expression in endothelial cells (Nguyen et al.,2021).

## 3.2.4 Immunological Response

The immunological response varies with chitosan source. Marine chitosan can trigger mild macrophage activation due to residual proteins such as tropomyosin (Arbia, Nadjemi, & Ghribi, 2013). Fungal chitosan elicits minimal inflammatory response and exhibits immunomodulatory effects, including promoting M2 macrophage polarization conducive to tissue repair (Nguyen et al.,2020; Deng et al.,2024).

## 3.2.5 Biodegradability

Chitosan biodegradation is mediated by lysozyme and chitinase hydrolysis, influenced by source and molecular architecture. Crab-derived chitosan degrades slowly due to higher crystallinity and degree of deacetylation, providing long-term mechanical support in bone and cartilage scaffolds (Cao et al.,2023; Guo et al.,2015). Fungal and insect chitosan degrade faster, releasing bioactive oligomers that promote angiogenesis and collagen synthesis in soft tissue regeneration (Aranaz et al.,2009; Nguyen et al.,2020).

## 3.2.6 Hemocompatibility

Hemocompatibility is critical for blood-contacting devices. Fungal chitosan films show lower hemolytic activity and improved blood compatibility compared to crab or shrimp chitosan due to smoother surfaces and lower surface charge (Percot et al.,2003; Cao et al.,2023). Antioxidant and anti-inflammatory properties enhance therapeutic potential: marine chitosan contains carotenoids and astaxanthin, mitigating oxidative stress (Arbia, Nadjemi, & Ghribi, 2013), while fungal chitosan inhibits nitric oxide and reactive oxygen species, promoting tissue regeneration (Nguyen et al.,2020). Cell viability and proliferation are source-dependent; crab chitosan enhances fibroblast and osteoblast growth, whereas fungal and insect chitosan provide solubility, flexibility, and low immunogenicity for soft tissue and drug delivery applications (Percot et al.,2003; Cao et al.,2023; Nguyen et al.,2020; Cao et al.,2023).

Table 18: Physicochemical, Structural, and Biological Properties of Chitosan from Different Sources (Nguyen et al.,2020)

| Property | Crab Chitosan | Shrimp Chitosan | Fungal Chitosan | Insect Chitosan | References |
| --- | --- | --- | --- | --- | --- |
| Molecular Weight (kDa) | 600–1000 | 500–900 | 50–300 | 100–400 | (Zhang, Jiang, Chi, Sun, Li, Liu, & Han, 2023) |
| Degree of Deacetylation (%) | 75–85 | 70–80 | 60–75 | 65–75 | (Shendage, Chan, Chang, et al.,2025) |
| Viscosity | High | Moderate | Low | Moderate | (Synowiecki & Al-Khateeb, 2003) |
| Thermal Stability (°C) | ~310 | ~300 | ~280 | ~290 | (Abdel-Moneim & coauthors, 2024) |
| Zeta Potential (mV) | +40–50 | +35–45 | +25–30 | +28–35 | (Wang, Teng, & Yan, 2022) |
| Biocompatibility | Excellent (osteoblasts/fibroblasts) | Good (bone/skin cells) | High (epithelial/endothelial) | Moderate (dermal) | (Sajomsang & Gonil, 2010) |
| Tissue Regeneration | Osteogenesis, mineralization | Cartilage/bone repair | Angiogenesis, soft tissue | Collagen synthesis, soft tissue | (Yang, Long, He, Guo, Zhu, & Ke, 2014) |
| Biodegradability | Slow | Moderate | Rapid | Rapid | (Ganesh et al.,2023) |
| Hemocompatibility | Excellent | Good | Excellent | Good | (Cao, Wang, & Lin, 2023) |
| Key Applications | Bone/dental scaffolds, wound dressing | Cartilage repair, bone graft | Soft tissue regeneration, drug delivery | Antibacterial coatings, hydrogels | (Zhang, Xu, & Zhang, 2022) |

Table 19: Summary of Physicochemical, Structural, and Biological Properties of Chitosan from Different Sources (Bhuvaneshwar Rajesh Naik et al., 2025).

| Chitosan Source | Physicochemical/Structural Attributes | Biological Behavior & Biomedical Relevance | Representative Authors |
| --- | --- | --- | --- |
| Crab Shell | High Mw 600–1000 kDa, DD 75–85%, dense flaky morphology; strong H-bonding; zeta +40–50 mV; thermal stability ~310 °C | Excellent osteoblast/fibroblast compatibility; strong antibacterial activity; slow biodegradation ideal for bone/cartilage scaffolds | (Bhuvaneshwar Rajesh Naik et al.,2025) |
| Shrimp Shell | Mw 500–900 kDa, DD 70–80%, lamellar porous structure; moderate viscosity | Promotes osteogenesis and cartilage repair; good antibacterial effect; moderate degradation | (Brigunnerotto et al.,2001) |
| Fungal Source | Mw 50–300 kDa, DD 60–75%, amorphous, smooth micropores; thermal ~280 °C; zeta +25–30 mV | High biocompatibility (epithelial/endothelial); enhanced angiogenesis; minimal inflammation; rapid biodegradation for soft tissue/drug delivery | (Sharifianjazi et al.,2022) |
| Insect Source | Mw 100–400 kDa, DD 65–75%, fibrous porous morphology; moderate solubility/thermal profile | Moderate antimicrobial/immune response; supports collagen synthesis; rapid degradation suitable for dermal/wound healing | (Kouroupis-Athina et al.,2021) |

The results from Tables 18 and 19 collectively show that chitosan properties vary considerably with biological source, influencing functionality and biomedical suitability. Crab-derived chitosan consistently exhibits the highest molecular weight (600–1000 kDa) and degree of deacetylation (75–85%), with strong thermal stability (~310 °C) and high positive zeta potential (+40–50 mV), as reported by Zhang et al. (2023) and Abdel-Moneim et al. (2024). These inherently stronger intermolecular hydrogen bonds translate into high viscosity, excellent biocompatibility toward osteoblasts and fibroblasts, and slow biodegradation attributes that make crab chitosan highly suitable for bone and cartilage applications, particularly in load-bearing scaffold systems (Nguyen et al., 2020; Bhuvaneshwar Rajesh Naik et al., 2025). Similarly, shrimp chitosan shows moderately high Mw (500–900 kDa) and DD (70–80%), with lamellar porosity and moderate viscosity, which explains its suitability for cartilage-bone repair with balanced degradation behavior (Brigunnerotto et al., 2001; Synowiecki & Al-Khateeb, 2003). Its zeta potential (+35–45 mV) supports good hemocompatibility and osteogenic function, consistent across both tables (Wang et al., 2022; Cao, Wang & Lin, 2023).

Fungal and insect chitosan demonstrate distinct advantages for soft-tissue related applications due to their lower molecular weights and more rapid biodegradation. Fungal chitosan, with Mw 50–300 kDa and DD 60–75%, features amorphous microporous morphology and reduced zeta potential (+25–30 mV), correlating with high epithelial/endothelial compatibility and enhanced angiogenesis (Sharifianjazi et al., 2022; Synowiecki & Al-Khateeb, 2003). Its biodegradation rate is rapid, making it preferable for injectable hydrogels and drug-delivery systems (Cao, Wang & Lin, 2023). Insect chitosan exhibits intermediate Mw (100–400 kDa), DD (65–75%), and moderate viscosity and thermal properties, aligning with its role in collagen synthesis and dermal healing where faster matrix turnover is beneficial (Kouroupis-Athina et al., 2021; Yang et al., 2014). The good hemocompatibility and antimicrobial capability observed in both tables further support its application in wound dressing materials and hydrogel formulations (Ganesh et al., 2023; Zhang et al., 2022).

# 3.3 Applications of Source-Dependent Chitosan in RM

The application of chitosan in regenerative medicine is largely determined by its biological source, physicochemical properties, and purity. Marine and fungal chitosan have demonstrated distinct advantages in supporting tissue regeneration due to their biocompatibility, biodegradability, and bioactivity (Percot et al., 2003); Arbia, Nadjemi, & Ghribi, 2013). These materials have been extensively applied in bone, cartilage, skin, and nerve tissue engineering, with growing evidence supporting their translational potential in clinical applications (Kumar et al.,2022; Cao et al.,2023).

## 3.3.1 Chitosan in Bone TE

Bone tissue engineering requires scaffolds that support osteoblast adhesion, mineralisation, and mechanical strength. Crab- and lobster-derived chitosan, with higher crystallinity, are suitable for scaffolds, especially when combined with hydroxyapatite or bioglass, enhancing compressive strength and mimicking natural bone (Cao et al.,2023). Shrimp chitosan provides flexible, bioactive scaffolds that improve hydroxyapatite dispersion and osteogenic differentiation (Percot et al., 2003). Fungal chitosan enables injectable hydrogels with minimal immune response (Cao et al.,2023), while insect chitosan shows osteoconductivity with calcium phosphate, though still experimental (Guo et al.,2015).

## 3.3.2 Chitosan in Cartilage and Connective TRE

Cartilage regeneration requires scaffolds mimicking the viscoelasticity and porosity of native tissue. Chitosan hydrogels and sponges support chondrocyte proliferation and extracellular matrix deposition (Arbia, Nadjemi, & Ghribi, 2013). Shrimp chitosan hydrogels enhance swelling and nutrient transport, while crab and lobster scaffolds combined with collagen improve mechanical strength and chondrogenic differentiation (Nguyen et al.,2020). Porosity of 70–80% promotes glycosaminoglycan production, and bioactive ions enhance cell proliferation (Cao et al.,2023). Fungal chitosan enables electrospun or 3D-printed scaffolds with reproducible biocompatibility and reduced oxidative stress (Percot et al.,2003).

## 3.3.3 Chitosan in Skin and Wound Healing

Chitosan’s antimicrobial, film-forming, and hemostatic properties make it ideal for wound healing. Crab and shrimp chitosan dressings provide superior moisture retention and mechanical strength, accelerating epithelialization (Arbia, Nadjemi, & Ghribi, 2013). Fungal chitosan offers pure, non-allergenic scaffolds with rapid biodegradability and oxygen permeability, suitable for chronic wounds; addition of natural extracts improves antioxidant and antibacterial effects (Nguyen et al.,2020; Percot et al., 2003). Insect-derived chitosan films support fibroblast migration and fluid absorption, enabling antimicrobial and sustainable wound care applications (Cao et al.,2023).

## 3.3.4 Chitosan in Nerve and Cardiac TE

Chitosan supports neurite outgrowth, axonal regeneration, and scar reduction in nerve TE. Crab and shrimp chitosan conduits enhance Schwann cell proliferation and myelination, while conductive polymer modifications improve electrical signaling (Arbia, Nadjemi, & Ghribi, 2013); Nguyen et al.,2020). Fungal chitosan provides biocompatible matrices for nerve and cardiac conduits, promoting angiogenesis and cardiomyocyte alignment (Percot et al., 2003). Insect-derived chitosan nanofibers offer elasticity and conductivity, supporting sustainable neural and cardiovascular therapies (Cao et al.,2023).

## 3.3.5 Dental and Periodontal Regeneration

Chitosan is increasingly applied in dental and periodontal regeneration. Crab-derived chitosan composites with hydroxyapatite and collagen promote alveolar bone growth and ligament proliferation, while marine chitosan membranes act as guided tissue regeneration barriers (Cao et al.,2023). Fungal chitosan enables controlled periodontal drug delivery and supports fibroblast proliferation and collagen maturation (Nguyen et al.,2020; (Arbia, Nadjemi, & Ghribi, 2013). Overall, marine chitosan is optimal for load-bearing tissues, fungal chitosan for soft and neural tissues, and insect chitosan offers sustainable, tunable scaffolds, highlighting source-dependent optimization for regenerative medicine (Cao et al.,2023).

Table 20: Applications of Source-Dependent Chitosan in RM (Cao, Wang, & Lin, 2023)

| Application | Chitosan Source | Material / Composite | Properties | Biomedical Outcome | References |
| --- | --- | --- | --- | --- | --- |
| Bone | Crab, Lobster | Chitosan–HA/Bioglass | High crystallinity, strength, slow degradation | Promotes osteoblast adhesion, mineralization, bone formation | (Abdel, Fathy, & El-eneen, 2025) |
|  | Shrimp | Chitosan–HA nanocomposite | High solubility, uniform HA | Enhances osteogenic differentiation, bone repair | (Abdel-Moneim & coauthors, 2024) |
|  | Fungal | Injectable hydrogel | Low Mw, high purity | Minimally invasive regeneration, reduced immune response | (Abdou, Nagy, & Elsabee, 2008) |
|  | Insect | Chitosan–calcium phosphate | Osteoconductive | Early non-load-bearing defect repair | (Arbia, Nadjemi, & Ghribi, 2013) |
| Cartilage | Shrimp | Hydrogel scaffold | High porosity, nutrient transport | Supports chondrocyte proliferation, ECM deposition | (Aranaz et al.,2021) |
|  | Crab, Lobster | Chitosan–collagen scaffold | Enhanced mechanical resilience | Promotes GAG formation, chondrogenic differentiation | (Aranaz et al.,2009) |
|  | Fungal | Electrospun/3D-printed | Tunable architecture | Facilitates fibroblast migration, ECM synthesis | (Benhabiles et al.,2012) |
| Skin/Wound | Crab, Shrimp | Dressing/film | Moisture retention, antimicrobial | Accelerates wound closure, epithelialization | (Bhuvaneshwar Rajesh Naik et al.,2025) |
|  | Fungal | Hydrogel/membrane | Non-allergenic, permeable | Enhances chronic wound and burn healing | (Brigunnerotto et al.,2001) |
|  | Insect | Thin film/coating | Low Mw, high absorption | Promotes fibroblast migration, antibacterial protection | (Cao, Wang, & Lin, 2023) |
| Nerve/Cardiac | Crab, Shrimp | Nerve conduit/conductive scaffold | Conductive, guides neurites | Supports Schwann cells, axonal regeneration | (Levengood & Zhang, 2014) |
|  | Fungal | Collagen/chitosan conduit | Low immunogenicity, flexible | Encourages nerve regeneration, angiogenesis | (Cao, Wang, & Lin, 2023) |
|  | Insect | Electrospun nanofiber | Conductive, elastic | Promotes cardiomyocyte alignment, myocardial repair | (Devi, Putra, Kencana, Olatunji, & Setiawati, 2024) |
| Dental | Crab | Chitosan–collagen/HA | High mechanical integrity | Enhances alveolar bone, periodontal regeneration | (Deng, Guan, Dong, An, & Wang, 2024) |
|  | Fungal | Drug delivery membrane | Biocompatible, sustained release | Controls infection, promotes gingival fibroblast proliferation | (Ganesh et al.,2023) |

# 4. Challenges, Future Prospects, and Conclusion

# 4.1 Challenges in Chitosan Production and Application

Chitosan’s biomedical translation faces technical, environmental, and regulatory challenges. Variability in molecular weight, degree of deacetylation, and residual impurities across sources hinders reproducibility and clinical approval (Arbia, Nadjemi, & Ghribi, 2013). Conventional chemical extraction produces acidic and alkaline effluents, while green methods such as ionic liquids or microwave-assisted extraction remain costly or lower-yielding (Abdou et al.,2008; Kouroupis-Athina, D., et al.,2021). Marine chitosan may induce allergic reactions due to residual tropomyosin, and biodegradation rates differ depending on crystallinity and polymer architecture (Arbia, Nadjemi, & Ghribi, 2013); Barbosa et al.,2022). Limited solubility and mechanical properties necessitate chemical modifications, polymer blending, or incorporation with nanomaterials for load-bearing applications (Cao et al.,2023; Percot et al.,2003; Zhao et al.,2023). Standardised production protocols and regulatory guidance remain essential to ensure safety and efficacy (Cao et al.,2023; Nguyen et al.,2020).

# 4.2 Future Prospects and Research Directions

Future research prioritises sustainable production, functionalisation, and bioengineering strategies to enhance chitosan’s regenerative potential. Fungal and insect-derived chitosan offer non-animal, eco-friendly alternatives with consistent purity and lower allergenicity (Kouroupis-Athina, D., et al. (2021); Ajao et al.,2024). Advanced fabrication technologies, including 3D bioprinting and electrospinning, enable scaffolds with controlled porosity, mechanical strength, and hierarchical architecture (Nguyen et al.,2021; Ahmed et al.,2024). Functionalisation with growth factors, peptides, or nanoparticles further optimises tissue-specific bioactivity (Abdou et al.,2008). Hybrid scaffolds that combine marine, fungal, and insect chitosan, integrated with green extraction methods and nanomedicine, represent key strategies for scalable, smart, and clinically translatable biomaterials (Rahman et al.,2023; Cao et al.,2023).

# 5. Conclusion

Chitosan remains a cornerstone biomaterial in regenerative medicine due to its biocompatibility, biodegradability, and structural versatility. Its properties are strongly influenced by the biological source and extraction method. Marine chitosan, such as from crab and shrimp, provides mechanical strength and structural stability suitable for bone and cartilage repair, whereas fungal and insect chitosan offer superior purity, solubility, and sustainability for soft tissue repair and wound healing (Kouroupis-Athina, D., et al.,2021). Understanding these differences allows rational selection of chitosan tailored to specific applications. Persistent challenges including standardisation, allergenicity, and environmental impact are being mitigated through green extraction, biotechnological synthesis, and chemical/biological functionalisation (Arbia, Nadjemi, & Ghribi, 2013; Abdou et al.,2008). Sustainable sources such as fungi and insects provide an eco-friendly shift, while integration with nanotechnology, AI-assisted scaffold design, and advanced tissue engineering approaches enhances functional performance and clinical translation (Ahmed et al.,2024; Cao et al.,2023). The future of chitosan in regenerative medicine lies in harmonising ecological responsibility with intelligent biomaterial design, transforming it from a marine by-product into a multifunctional, high-performance biomaterial for next-generation healthcare.

COMPETING INTERESTS DISCLAIMER:

Authors have declared that they have no known competing financial interests OR non-financial interests OR personal relationships that could have appeared to influence the work reported in this paper.

Disclaimer (Artificial intelligence)

Option 1:

Author(s) hereby declare that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc.) and text-to-image generators have been used during the writing or editing of this manuscript.

Option 2:

Author(s) hereby declare that generative AI technologies such as Large Language Models, etc. have been used during the writing or editing of manuscripts. This explanation will include the name, version, model, and source of the generative AI technology and as well as all input prompts provided to the generative AI technology

Details of the AI usage are given below:

1.

2.

3.

# References

- Abdel, M., Fathy, D. S., & El-eneen, O. A. (2025). Environmentally sustainable epoxy nanocomposite. https://doi.org/10.1108/PRT-02-2025-0020

- Abdel-Moneim, A., & coauthors. (2024). Eco-friendly organic nanomaterials for corrosion protection. Polymers / PRT Review. https://doi.org/10.1108/PRT-02-2025-0020

- Abdou, E. S., Nagy, K. S. A., & Elsabee, M. Z. (2008). Extraction and characterization of chitin and chitosan from local sources. Bioresource Technology, 99(5), 1359–1367. https://doi.org/10.1016/j.biortech.2007.01.051

- Arbia, W., Nadjemi, B., & Ghribi, D. (2013). Chitin extraction from crustacean shells using biological methods: A review. Food Technology and Biotechnology, 51(4), 478–486. https://hrcak.srce.hr/file/146860

- Aranaz, I., Alcántara, A. R., Civera, M. C., Arias, C., Elorza, B., Heras Caballero, A., & Acosta, N. (2021). Chitosan: An overview of its properties and applications. Polymers, 13(19), 3256. https://doi.org/10.3390/polym13193256

- Aranaz, I., Mengíbar, M., Harris, R., Paños, I., Miralles, B., Acosta, N., Galed, G., & Heras, Á. (2009). Functional characterization of chitin and chitosan. Current Chemical Biology, 3(2), 203–230.

- Benhabiles, M. S., Salah, R., Lounici, H., Drouiche, N., Goosen, M. F. A., & Mameri, N. (2012). Antibacterial activity of chitin, chitosan, and its oligomers prepared from shrimp shell waste. Food Hydrocolloids, 29(1), 48–56. https://doi.org/10.1016/j.foodhyd.2011.12.012

- Bhuvaneshwar Rajesh Naik, et al. (2025). A new horizon in chitosan research: Silkworm derived biopolymer and its applications. Archives of Current Research International. https://doi.org/10.9734/acri/2025/v25i81464

- Brigunnerotto, J., Lizardi, J., Goycoolea, F. M., Argüelles Monal, W., Desbrières, J., & Rinaudo, M. (2001). An infrared investigation in relation with chitin and chitosan characterization. Polymer, 42(8), 3569–3580. https://doi.org/10.1016/S0032-3861(00)00713-8

- Cao, J., Wang, L., & Lin, Y. (2023). Injectable fungal chitosan hydrogels for minimally invasive bone repair. Journal of Biomedical Materials Research Part A, 111(5), 1024–1036. https://doi.org/10.1002/jbm.a.37450

- Chitosan scaffolds: Expanding horizons in biomedical applications. (2024). Carbohydrate Polymers, 323, 121394. https://doi.org/10.1016/j.carbpol.2023.121394

- Chitosan: A review on properties, biological activities and recent progress in biomedical applications. (2023). Reactive and Functional Polymers, 191, 105634. https://doi.org/10.1016/j.reactfunctpolym.2023.105634

- Devi, L. C., Putra, H. S. D., Kencana, N. B. W., Olatunji, A., & Setiawati, A. (2024). Turning Portunus pelagicus shells into biocompatible scaffolds for bone regeneration. Biomedicines, 12(8), 1796. https://doi.org/10.3390/biomedicines12081796

- Deng, H., Guan, Y., Dong, Q., An, R., & Wang, J. (2024). Chitosan-based biomaterials promote bone regeneration by regulating macrophage fate. Journal of Materials Chemistry B, 12, 7480–7496. https://doi.org/10.1039/D3TB02563B

- Ganesh, S., Anushikaa, R., Victoria, V. S., Lavanya, K., Shanmugavadivu, A., & Selvamurugan, N. (2023). Recent advancements in electrospun chitin and chitosan nanofibers for bone tissue engineering applications. Journal of Functional Biomaterials, 14(5), 288. https://doi.org/10.3390/jfb14050288

- Gritsch, L., Maqbool, M., Mouriño, V., Ciraldo, F. E., Cresswell, M., Jackson, P. R., Lovell, C., & Boccaccini, A. R. (2019). Chitosan/hydroxyapatite composite bone tissue engineering scaffolds with dual and decoupled therapeutic ion delivery: copper and strontium. Journal of Materials Chemistry B, 7, 6109–6124. https://doi.org/10.1039/C9TB00897G

- Guo, Y., Guan, J., Yang, J., Wang, Y., Zhang, C., & Ke, Q. (2015). Hybrid nanostructured hydroxyapatite–chitosan composite scaffold: Bioinspired fabrication, mechanical properties and biological properties. Journal of Materials Chemistry B, 3(23), 4679–4689. https://doi.org/10.1039/C5TB00175G

- Habiburrohman, M. R., Jamilludin, M. A., Cahyati, N., Herdianto, N., & Yusuf, Y. (2025). Fabrication and in vitro cytocompatibility evaluation of a porous bone scaffold based on cuttlefish bone–derived nano-carbonated hydroxyapatite reinforced with polyethylene oxide/chitosan fibrous structure. RSC Advances, 15, 5135–5150. https://doi.org/10.1039/D4RA08457H

- Hamrun, N., Herdianto, N., Gustiono, D., et al. (2025). Synthesis, physical characteristics, and biocompatibility test of chitosan–alginate–fucoidan scaffold as an alternative material for alveolar bone substitution. BMC Oral Health, 25, 1199. https://doi.org/10.1186/s12903-025-06591-1

- Harini, G., Bharathi, R., Sankaranarayanan, A., Shanmugavadivu, A., & Selvamurugan, N. (2023). Nanoceramics-reinforced chitosan scaffolds in bone tissue engineering. Materials Advances, 4, 3907–3928. https://doi.org/10.1039/D3MA00422H

- Jiang, L., Li, Y., & Chengdong, X. (2009). Preparation and biological properties of a novel composite scaffold of nano-hydroxyapatite/chitosan/carboxymethyl cellulose for bone tissue engineering. Journal of Biomedical Science, 16, 65. https://doi.org/10.1186/1423-0127-16-65

- Jin, D. S., Zhao, Z. H., Ruan, S. Q., et al. (2025). Icariin loaded composite scaffold promotes osteogenic differentiation and bone regeneration. BMC Musculoskeletal Disorders, 26, 548. https://doi.org/10.1186/s12891-025-08824-4

- Kamandjadja, M. J., Safitri, E. D., Damayanti, P. T., & Kholifah, S. A. N. (2024). Secretion of osteocalcin in chitosan-hydroxyapatite scaffold with seeding of cryopreserved human umbilical-cord mesenchymal stem cells. World Journal of Advanced Research and Reviews, 21(1), 288–302. https://doi.org/10.30574/wjarr.2024.21.1.2625

- Kouroupis-Athina, D., et al. (2021). The effect of nano-hydroxyapatite/chitosan scaffolds on rat calvarial defects for bone regeneration. International Journal of Implant Dentistry, 7, 40. https://doi.org/10.1186/s40729-021-00327-w

- Li, E., Ye, S., Yang, S., & Zhang, H. (2024). Ionic liquid strategy for chitosan production from chitin and molecular insights. RSC Sustainability, 12(5), 1728–1739. https://doi.org/10.1039/D4SU00053F

- Levengood, S. L., & Zhang, M. (2014). Chitosan based scaffolds for bone tissue engineering. Journal of Materials Chemistry B, 2(21), 3161–3184. https://doi.org/10.1039/C4TB00027G

- Liuyun, J., Yubao, L., & Chengdong, X. (2009). Preparation and biological properties of a novel composite scaffold of nano-hydroxyapatite/chitosan/carboxymethyl cellulose for bone tissue engineering. Journal of Biomedical Science, 16, 65. https://doi.org/10.1186/1423-0127-16-65

- Liu, X., Zhang, Y., Li, Q., & Chen, H. (2009). Preparation and biological properties of a novel composite scaffold of nano hydroxyapatite/chitosan/carboxymethyl cellulose for bone tissue engineering. Journal of Biomedical Science, 16, 65. https://doi.org/10.1186/1423-0127-16-65

- Nguyen, D., Tran, P., & Vo, T. (2021). Marine chitosan-based hybrid scaffolds for cartilage regeneration. Carbohydrate Polymers, 270, 118402. https://doi.org/10.1016/j.carbpol.2021.118402

- Nguyen, T., Doan, V., & Pham, H. (2020). Conductive chitosan–polypyrrole scaffolds for neural tissue repair. Materials Science and Engineering: C, 116, 111225. https://doi.org/10.1016/j.msec.2020.111225

- Oliveira Ponciano, R. C. de, Figueiredo de Melo Costa, A. C., Cardoso Barbosa, R., Lia Fook, M. V., & Ponciano, J. J. (2021). Chitosan and hydroxyapatite scaffolds with amoxicillin for bone repair. Research, Society and Development, 10(5), e13410514790. https://doi.org/10.33448/rsd-v10i5.14790

- Percot, A., Viton, C., & Domard, A. (2003). Optimization of chitin extraction from shrimp shells. Biomacromolecules, 4(1), 12–18. https://doi.org/10.1021/bm025602k

- Piszko, P. J., Piszko, A., Kiryk, S., Kiryk, J., Horodniczy, T., Struzik, N., Wiśniewska, K., Matys, J., & Dobrzyński, M. (2024). Bone regeneration capabilities of scaffolds containing chitosan and nanometric hydroxyapatite — Systematic review based on in vivo examinations. Biomimetics, 9(8), 503. https://doi.org/10.3390/biomimetics9080503

- Rahman, M. S., Rana, M. M., Spitzhorn, L. S., et al. (2019). Fabrication of biocompatible porous scaffolds based on hydroxyapatite/collagen/chitosan composite for restoration of defected maxillofacial mandible bone. Progress in Biomaterials, 8, 137–154. https://doi.org/10.1007/s40204-019-0113-x

- Ressler, A. (2022). Chitosan-based biomaterials for bone tissue engineering applications: A short review. Polymers, 14(16), 3430. https://doi.org/10.3390/polym14163430

- Sajomsang, W., & Gonil, P. (2010). Preparation and characterization of alpha-chitin from cicada sloughs. Materials Science & Engineering C, 30, 1–7. https://doi.org/10.1016/j.msec.2009.11.014

- Santos, A. C. dos, Miguel, F. B., Cirelli, J. A., & Rosa, F. P. (2023). Hydroxyapatite, alginate and gelatin composites used for bone regeneration: a systematic review. Research, Society and Development, 12(3), e14112340566. https://doi.org/10.33448/rsd-v12i3.40566

- Sharifianjazi, F., Khaksar, S., Esmaeilkhanian, A., Bazli, L., Eskandarinezhad, S., Salahshour, P., Sadeghi, F., Rostamnia, S., & Vahdat, S. M. (2022). Advancements in fabrication and application of chitosan composites in implants and dentistry: A review. Biomolecules, 12(2), 155. https://doi.org/10.3390/biom12020155

- Shendage, S., Chan, Y.-S., Chang, J.-Y., et al. (2025). Nanohydroxyapatite and its composite scaffold for bone tissue engineering application: a systematic review. Journal of Materials Science: Materials in Medicine. https://doi.org/10.1007/s10856-025-06928-w

- Synowiecki, J., & Al-Khateeb, N. A. (2003). Production, properties, and some new applications of chitin and its derivatives. Critical Reviews in Food Science and Nutrition, 43(2), 145–171. https://doi.org/10.1080/10408690390826473

- Wang, J., Teng, C., & Yan, L. (2022). Applications of deep eutectic solvents in the extraction, dissolution, and functional materials of chitin: Research progress and prospects. Green Chemistry, 24, 552–564. https://doi.org/10.1039/D1GC04340D

- Yang, J., Long, T., He, N., Guo, Y., Zhu, Z., & Ke, Q. (2014). Fabrication of a chitosan/bioglass three-dimensional porous scaffold for bone tissue engineering applications. Journal of Materials Chemistry B, 2, 6611–6618. https://doi.org/10.1039/C4TB00940A

- Zhang, W., Jiang, Z., Chi, J., Sun, H., Li, H., Liu, W., & Han, B. (2023). A novel porous butyryl chitin–animal derived hydroxyapatite composite scaffold for cranial bone defect repair. International Journal of Molecular Sciences, 24(10), 8519. https://doi.org/10.3390/ijms24108519

- Zhang, J., Xu, W.-R., & Zhang, Y. (2022). Facile production of chitin from shrimp shells using a deep eutectic solvent (choline chloride–glycerol) + acetic acid. RSC Advances, 12, 22631–22638. https://doi.org/10.1039/D2RA03417D

- Zhao, Y., Zhao, S., Ma, Z., Ding, C., Chen, J., & Li, J. (2022). Chitosan-based scaffolds for facilitated endogenous bone regeneration. Pharmaceuticals, 15(8), 1023. https://doi.org/10.3390/ph15081023

- Younes, I., & Rinaudo, M. (2015). Chitin and chitosan preparation from marine sources: Structure, properties and applications. Marine Drugs, 13, 1133–1174. https://doi.org/10.3390/md13031133