Self-Healing Polymer Composites from Waxy Maize Starch: Mechanisms and Sustainable Applications

ABSTRACT

Herein, we reviewed a highly branched, amylopectin-rich biopolymer, waxy maize starch (WMS), which promises to be a good matrix for durable self-healing polymer composites

Brittle petroleum-based polymers and native starch films lack barrier properties and self-healing. Sustainable alternatives are needed. In its high amylopectin concentration and unusual branching structure, waxy maize starch (WMS) may be a renewable resource for self-healing polymer composites. This article discusses WMS-based self-healing composite material design, healing processes, and sustainable applications. Advanced technologies include enzymatic branching, dynamic borate ester bonding, nanocrystal reinforcement, and microcapsule-assisted healing have enhanced mechanical strength, healing efficiency, and functional performance. Various reviews reveal that WMS composites can recover over 58% of their mechanical integrity after damage, indicating its practicality. These findings demonstrate WMS as a scalable, renewable platform for next-generation green materials and suggest self-healing biopolymer research.This review examines waxy maize starch-based polymer composite design, self-healing, and sustainable applications.

Keywords: polymer composites, self-healing, mechanism, starch

1.0 INTRODUCTION

The environmental effect of traditional materials and the need for sustainable alternatives have become more apparent in recent years. Self-healing materials have transformed building and infrastructure by increasing durability and lifespan. Self-repairing micro-cracks in concrete and cementitious composites minimise maintenance costs and environmental effects [1].

Based on this idea, self-healing polymer composites are becoming sustainable packaging, coatings, and functional films. Among bio-based polymers, starch is renewable, biodegradable, and chemically flexible for dynamic healing networks.

Starch, a natural polymer characterised by its abundant availability, cost-effectiveness, renewability, and full biodegradability, is one of the most promising and applicable natural degradable materials [2–4].

There are three categories of starch based on amylose concentration: native starch (15-30 wt% amylose), waxy starch (0-5 wt% amylose), and high amylose starch (35-70 wt% amylose) [5, 6]

More so, Starch granules consist of linear amylose and branching amylopectin macromolecules in varying ratios depending on their source and classification.  Normal maize starch (25% amylose, 75% amylopectin), waxy maize starch (0–2% amylose, 98% amylopectin), and amylose-starch (up to 70% amylose) exemplify several maize starch varieties characterised by distinct amylose and amylopectin ratios [7]. When starch dispersion is heated to its gelatinisation temperature with water and a plasticiser like glycerol, the resultant films exhibit brittleness and inferior mechanical and barrier properties [8].

High amylopectin concentration in waxy maize starch creates a highly branched structure for flexible films and rapid self-repair. It generates reversible bonding networks that can self-heal mechanical damage when paired with green, plant-derived cross-linkers like tannic acid or citric acid. Waxy maize starch nanocrystals, hydrolysed from native granules, reinforce thermoplastic starch and demonstrate remarkable reinforcing and barrier capabilities in natural rubber [9, 10]

Starch-based composites improve material durability and minimise environmental impact, supporting circular economy and green chemistry. Bio-based polymers and self-healing systems have advanced, but waxy maize starch in self-healing polymer composites for sustainable applications has not.

Despite interest in bio-based self-healing materials, waxy maize starch (WMS) in polymer composites has not been systematically investigated.This  paper discusses waxy maize starch-based self-healing polymer composites' design, healing mechanisms, structure-property linkages,and applications.  It addresses mechanical strength, healing efficiency, processing issues, and environmental stability, offering scalable and sustainable packaging and functional film solutions.

Review Methodology

This review method involved searching Scopus, Web of Science, and Google Scholar for relevant publications from 2000-2025 using keywords such ‘waxy maize starch’, ‘self-healing polymer’, and ‘sustainable composites.  Selected publications were carefully analysed to summarise mechanisms, material features, and applications after relevant screening

2.0 THE SELECTION OF MATRIX

Self-healing starch-based composites' mechanical strength, self-healing efficiency, processability, and application potential depend on the matrix. Recent researches suggest the following matrix selection criteria.

Table 1: Type of matrix and its composition, mechanism and tailored advantages

| Type of Matrix | Composition | Mechanism | Advantages | References |
| --- | --- | --- | --- | --- |
| Modified Starch, Imine Networks Thermoplastics | Fully biodegradable, thermally processable starch plastics with dynamic imine linkages | Reversible imine bonds self-repair at heat or mild pressure. | Durable, recyclable, thermally processable, biodegradable | [11] |
| Borax-crosslinked starch-acrylamide hydrogels | Acrylamide-grafted starch; borax crosslinker | Reversible borate ester linkages enable self-healing. | Flexible, good water retention, adjustable mechanical characteristics | [12] |
| Starch-synthetic polymer double-network hydrogels | Starch and synthetic polymer (e.g., polyacrylamide) interpenetrating networks | Polymer entanglement + hydrogen bonding | Strong mechanical strength, about 99% self-healing. | [13] |
| CNC Starch/PVA/Nanocellulose Conductive Hydrogel | Dynamic borate/hydrogen bonding; starch, PVA, cellulose nanocrystals | 2-reversible cross-links | Mechanical strength, stretchability, self-healing, conductivity | [14] |
| Starch and MXene Nanosheet Hydrogel | Starch with MXene nanosheets and multi-bond network | Multi-reversible hydrogen-coordination bonds | Stretchable, self-healing, conductive; improved function | [15] |
| Tea/PVA/Starch Polyphenol Organohydrogel | Mixed starch, PVA, and polyphenols | Hydrogen-bonded reversible borate ester | Fast-healing, sticky, anti-freezing, antibacterial, multi-responsive | [16] |
| Thermoset Zein Composites | Biopolymer-based, rigid | High – WMS acts as biodegradable healing agent | Brittle, processing complexity | [17] |

Table 1 shows many matrix types suitable with waxy maize starch (WMS) for self-healing composites. Dynamic imine linkages allow modified starch thermoplastics to self-repair and recycle, making them suitable for sustainable packaging. Starch-acrylamide and double-network hydrogels use reversible borate ester or hydrogen bonding for variable mechanical strength and near-complete self-healing. Nanofillers (CNCs, MXene) improve mechanical robustness, conductivity, and stretchability, whereas starch/PVA/polyphenol organohydrogels heal quickly and are multi-responsive, making them useful for smart packaging or functional films. The table shows that matrix selection balances mechanical performance, self-healing efficiency, and application-specific needs. These findings suggest WMS is a potential biodegradable matrix for robust self-healing polymer composites.

Eco-friendly biodegradable films created from natural polymers can replace petroleum-based food packaging plastics [18–21]. Starch is a promising sustainable material due to its cost-effectiveness, biodegradability, and abundance [22–25]

The structural difference of different starches greatly affects film performance.  High-amylose starches make better oxygen barriers and mechanically stable films, especially at high humidity [28, 29]. However, amylopectin-only films are commonly amorphous [32, 33].

Strategic alteration and mixing can make high-performance films from waxy starches, which are essentially completely amylopectin. High-amylose starches have structural benefits.  Synthetic polymers like polyvinyl alcohol can make native starch films less brittle and more mechanically efficient.  Due to its many hydroxyl groups, Poly Vinyl Alcohol (PVA) is compatible with starch and improves composite film tensile strength and elongation [8, 34–39].

Figure 1. The self-healing capability of a renewable and biodegradable starch hydrogel [40]

3.0 POLYMER COMPOSITES

To solve petroleum-based resin sustainability and disposal difficulties, green composites produced from plant-based proteins, polysaccharides, oils, and other agricultural products have been created [41, 42]. Zein protein from maize includes functional sites like amine, carboxyl, and hydroxyl that may be exploited to generate crosslinks to create thermoset resins with improved mechanical qualities [43–46]. However, thermoset zein resins are brittle and crack-prone [47, 48]. Plasticisers and tougheners minimise brittleness but cannot prevent service failure [49–51]

Continuous stress generates microcracks in resins and composites, reducing mechanical characteristics and causing early failure [52, 53]. Self-healing polymers fix micro-damages autonomously [53, 54]. Synthetic polymers have microcapsule (MC)-based, microvascular, and intrinsic self-healing mechanisms [41, 55], with MC-based systems being the best.  MC-based systems contain resin-dispersed polymer microcapsules with healing ingredients.  Microcapsules shatter upon microcracks, releasing the healing ingredient to mend the resin [56]. Certain studies indicate self-healing green thermoplastic composites[41, 52, 57–59].

Self-healing microcapsules are usually made by emulsification-solvent evaporation. Kim and Netravali effectively encapsulated waxy maize starch (WMS) in poly-lactic-co-glycolic acid (PLGA) shells using water-in-oil-in-water (w/o/w) emulsification [41, 43].  PLGA's low brittleness, fracture toughness, biodegradability, and hydrolytic instability make it a desirable green shell polymer [60].

3.1 DESIGN OF COMPOSITES AND THE GREEN SYNTHESIS

Designing high-performance starch-based materials requires composite design, not simple formulas.  This requires deliberately mixing a starch matrix with reinforcing fillers and functional additives to overcome native starch's mechanical strength and barrier characteristics [61–65].

3.1.1 REINFORCING WITH NANOCRYSTAL FILLERS:

Fillers increase starch film mechanical characteristics.  Because they can be made from starch, starch nanocrystals are biodegradable and chemically compatible. This process is divided into two viz:

- Chemical reinforcement: A thermoplastic starch study employed waxy maize starch nanocrystals made by acid hydrolysis of natural starch granules.  Filler and matrix have comparable chemical structures; therefore, they establish strong hydrogen bonds [66]. This increases mechanical strength and delays starch matrix ageing and recrystallisation [66].

- Stabilised Nanofillers: Starch nanoparticles work well but clump in water. Waxy maize starch nanoparticles (WMSNs) were stabilised using κ-carrageenan (KC), a natural food gum, to address this issue [67–69]. A starch film with this WMSNs/KC filler has higher tensile strength and water vapour barrier [70].

3.1.2 ADVANCED CROSSLINKING STRATEGIES

Crosslinking strengthens the starch gel network, although results vary.  The unique "ionic synergistic multiple crosslinking" method greatly improves gel characteristics [71]. This process involve:

- Synergy Effect: This process uses citric acid, etherifying crosslinkers, and Ca²⁺ ions from calcium citrate. Wei and his team highlighted that competing interactions may make utilising two crosslinkers wasteful [71].  Therefore, adding Ca²⁺ ions have a synergistic effect [72, 73].

- Mechanism: Electrostatic interactions between Ca²⁺ cations and starch molecules improve crosslinking efficiency and efficacy [73–75]. The gel's thick, porous honeycomb structure resists deformation and is stronger [71, 76–78].

3.1.3 UTILISING FUNCTIONAL INGREDIENTS

Composite design can combine antibacterial activity to structural integrity, providing "active" materials for food packaging.

- Antimicrobial:  Salicylic acid (SA), a harmless, plant-derived chemical, may be added directly to starch-based films to boost antibacterial capabilities [70, 79–92].

- Proven Effectiveness: SA-containing films performed well against E. coli, S. aureus, and B. subtilis food pollutants.  Its potential for active food packaging was shown when the SA-infused film prevented bacterial growth and increased the shelf life of yoghurt compared to a regular film [70] .

4.0 SELF-HEALING MECHANISMS IN STARCH SYSTEMS

Figure 2: Method and Mechanism of Synthesis of Borax Cross-Linked Acrylamide-Grafted Starch Hydrogels [40]

Dynamic linkages can make starch-based hydrogels self-heal. These linkages may be broken and restored, allowing the material to heal itself.  The main processes include dynamic covalent bonding and noncovalent bonds [93–104]. This involves the following factors as stated by researchers:

- Dynamic Borate Ester Bonds:  This mechanism is key.  Reversible cross-linker borax dissociates in water to create borate ions.  These ions generate dynamic and reversible ester linkages with starch molecules' numerous hydroxyl groups [12, 105–108]. Cutting or breaking the hydrogel breaks these bonds.  When broken surfaces are reconnected, ester bonds can rebuild without external stimulus, "healing" the structure and restoring its mechanical qualities [12].

- Hydrogen bonding: The hydrogel network's self-healing characteristics come from borate ester bonds and hydrogen bonds [12]According to the study, hydrogen bonding alone are less successful at healing.  Hydrogel samples constructed without borax, which depended primarily on hydrogen bonding, only partially restored mechanical integrity after injury [12].

These dynamic borate ester linkages and hydrogen bonds offer the hydrogel extraordinary recovery and temperature responsiveness.  After extreme strain broke down the hydrogel's structure, rheological testing showed that the dual-bond system worked promptly to restore its stability [12].

Additionally, utilising a Double-network (DN) hydrogel improves starch reinforcement to build strong, self-healing materials.  These hybrid hydrogels have a chemically crosslinked network of poly acrylic acid (PAA) and 2-acrylamido-2-methyl-1-propanesulfonic acid (AMPS) and a physical network of gelatinised cassava starch.  Starch increases mechanical characteristics, resulting in a tensile strength above 200 kPa and excellent stretchability and flexibility.  This stable chemical network and dynamic physical network allow the composite gel to heal up to 99% after 24 hours at ambient temperature [13].

Although microcapsules are not mentioned, in the study by [109–111]reveals that inherent dynamic connections underlie the self-healing mechanism.  Gelatinised starch creates a huge network of reversible physical interactions, mostly hydrogen bonding and chain entanglements, that heals. Branching starch chains can reorganise and rejoin across the cracked interface of a damaged hydrogel, repairing noncovalent connections and restoring structure [13, 110, 111]. Hence it emphasises that starch gelatinisation and ethanol treatment increase the material's excellent self-healing capabilities by enhancing physical interactions [13, 112].

4.1 Self-Healing Mechanisms in Starch-Based Systems

Polymers and hydrogels made from starch use the high density of hydroxyl (–OH) groups on glucose units to produce dynamic, reversible networks.  Borate ester bonds, formed by borate ions (B(OH)\₄⁻) reacting with diol moieties on neighbouring starch chains, are a frequent and efficient method. These borate ester connections can dissociate under stress or swelling and re-form when the injured surfaces are brought back into touch (e.g., under mild pressure or under ambient temperatures), restoring network integrity.  Hydrogels produced from acrylamide grafted starch + borax entirely regained its storage modulus after being severed and reconnected, demonstrating that dynamic borate ester + hydrogen bonding networks enable reliable self-healing [113]

In hydrated, flexible systems, non-covalent interactions including hydrogen bonding, physical entanglement, and van der Waals forces are important.  A hybrid double network (DN) hydrogel with starch and secondary polymer networks achieved tensile strength >200 kPa and nearly 99% healing efficiency after 24 hours at room temperature, thanks to its dense hydrogen bond reinforced physical network [13].  DN or interpenetrating network designs combat the brittleness of single network starch hydrogels and balance mechanical strength with self-healing  [114].

However, trade-offs must be considered while creating self-healing starch composites.  Dynamic borate or hydrogen bonds aid healing, but moisture, pH, and ionic strength weaken crosslinks or expand the matrix, lowering barrier or mechanical performance.  Fillers or reinforcing agents (e.g., nanocellulose, nanofibers, other polymers) can increase strength and film integrity, but excessive stiffness or inadequate interfacial bonding may hinder chain movement needed for healing.  To maximise durability and self-repairability, starch's intrinsic hydroxyl rich chemistry (for healing) must be balanced with network architecture (single versus DN), crosslink density, and additive/filler loading.

5.0 THE SELF-HEALING SYSTEM OF WAXY MAIZE STARCH

The study conducted by [17] strongly supports enzyme-treated waxy maize starch (WMS) as a better biodegradable film self-healing agent.  Researchers changed normal WMS by sequentially treating α-amylase and transglucosidase, resulting in "enzyme-treated waxy maize starch" (EWMS) with higher branching degree (21.88%) and decreased viscosity [17]. This EWMS was encapsulated and implanted in a starch film matrix.  These capsules break when a microcrack occurs, allowing EWMS to flow into the injured region and chemically react to rebuild the film's structure [17, 115–117]. The results prove that enzymatic alteration works.  The modified EWMS microcapsules improved film healing efficiency by 58.33%, compared to 44.65% for untreated WMS films.  The EWMS's reduced viscosity and more active reaction sites made crack mending more successful.  Thus, better-healed films had reduced water vapour permeability, indicating a more compact and repaired structure.  The study concludes that increasing WMS branching and fluidity creates a more powerful self-healing agent [17]

Table 2: A Summary of previous studies on starch-based self-healing / composites

| Materials | Composition | Observations | Relevances | References |
| --- | --- | --- | --- | --- |
| Hydrogel from acrylamide-grafted generic starch | Dynamic crosslinker borax | Hydrogel exhibits reversible self-healing via borate ester + H bonding, enhanced storage modulus ~1.8×, and thermal responsiveness | Proving that starch + dynamic borate crosslinking may create mechanically strong, self-healing hydrogels is important for WMS-based systems. | [118] |
| Corn-starch hydrogel | Borax (dynamic), twofold network. | Ideal for self-healing and form restitution after injury, with compression strength of ≈288kPa (10× pure starch hydrogel). | Shows double network + dynamic crosslink toughness + healing—inspires WMS-based composite construction. | [114] |
| Starch/PVA/CNCs hydrogel | Borax + nanocellulose filler | Self-healing and remoulding at room T; dual reversible bonding (borate + H bond), enhanced mechanical strength, conductivity, and stretchability. | Combines nanocellulose, starch, and dynamic bonding to create multifunctional self-healing composites for reinforced WMS composites. | [14] |
| Amylopectin-based starch + PVA + MXene nanosheets (hydrogel) | Nanofiller MXene, borate/H bond network | Excellent stretchability (~6151%), electrical conductivity, self-healing, and stickiness, with multifunctional potential for skin and sensors. | Advanced composite with excellent performance from dynamic bonding and nanofiller reinforcement—relevant template for WMS-based functional materials. | [15] |

Dynamic covalent bonding, double-network architectures, fillers, and conductive or nanofiller composites are used in self-healing starch-based polymer composite research. Despite these advances, few research has examined waxy maize starch (WMS) as a self-healing agent or WMS-based films or packaging. This gap allows for additional research into WMS-specific self-healing composites, which might improve durability and biodegradability. This review is innovative and practical.

5.1 WMS MICROCAPSULES IN SELF-HEALING COMPOSITES

[119] Souzandeh and Netravali introduced waxy maize starch (WMS) as a biodegradable healing agent in thermoset zein composites.  Using a unique co-axial injection approach, they encased WMS in PLGA shells to construct elongated multi-geometrical microcapsules with aspect ratios >1.  The capsules broke and released WMS that crosslinked with excess glutaraldehyde in the resin to build bridges over microcracks in the composite, restoring structural integrity.  With 15wt% WMS/PLGA microcapsules at room temperature, the system self-healed 51% in 24 hours. The researchers improved performance by oxidising WMS with sodium periodate to generate aldehyde functional groups, oxidised waxy maize starch (OWMS), which allowed covalent connection with zein's amine groups instead of hydrogen bonding.  The redesigned WMS improved self-healing efficacy by 42% with 15wt% OWMS/PLGA loading to 72%.  Compared to spherical capsules, elongated capsules had rougher surfaces and a greater microcrack path probability, which improved mechanical bonding with resin.  This totally bio-based technology shows that agricultural starches may repair autonomously, providing a sustainable alternative to petroleum-based products[119]

Table 3: Composite systems, Additives and their key results

| Composite system | Additives | Results | References |
| --- | --- | --- | --- |
| Acid-hydrolyzed WMS nanocrystal | WMS nanocrystals (no synthetic polymer) | Conversion of WMS granules into parallelepiped nanocrystals indicates that WMS can produce stable nano reinforcing structures. | [120] |
| Pregelatinized WMS/PVA mix films | Sorbitol/cardanol oil film-casting plasticisers | Improved tensile strength (~11% after pre-gelatinization) and thermal stability, proving WMS-based film feasibility for biodegradable packaging. | [121] |
| WMS nanoparticles/κ carrageenan (WMSNs/KC) + salicylic acid composite films | Antimicrobial, WMS nanofillers (WMSNs/KC) | Films have better tensile strength, water vapour barrier, thermal stability, and antibacterial activity against E. coli, S. aureus, and B. subtilis, demonstrating functional possibilities beyond structural films. | [70] |  |

The research presented propose a versatile “toolbox” for improving starch-based films and composites in various applications, including nanofiller reinforcement (e.g. nanocellulose/microcrystalline cellulose), polymer mixing, and chemical/physico chemical alterations.  Biodegradable, UV absorber, and thermal stable bioplastic films from waxy corn starch/polyvinyl alcohol blends show that WMS blended with PVA and plasticisers can increase tensile strength, thermal stability, and UV blocking, supporting its use as a sustainable packaging base [121]. Starch films reinforced with nanocellulose or microcrystalline cellulose have better mechanical strength and barrier properties [122].

6.0 APPLICATIONS OF WMS IN SUSTAINABLE PACKAGING AND FUNCTIONAL FILMS

Waxy maize starch (WMS) is a potential biodegradable packaging material that degrades completely while keeping functionality.  After 21 days, modified waxy maize starch films mixed with polyvinyl alcohol and plasticised with sorbitol-cardanol combinations degrade 95.5% and lose 96% of their weight [121]. These coatings can safeguard light-sensitive food products by absorbing up to 69% of UV rays [121, 123]. The increased thermal stability, with degradation temperatures reaching 318°C, and tensile strength by pre-gelatinization make these materials viable alternatives to petroleum-based packaging [121, 124, 125].

Antimicrobial starch-based composite films increase food preservation active packaging technology.  New films containing salicylic acid (SA) and WMSNs/KC show strong antibacterial action against E. coli, S. aureus, and B. subtilis, with inhibition zones of 52-56 mm. WMSNs/KC nanofillers improve tensile strength, water vapour barrier, and film transparency.  Application on yoghurt samples showed strong bacteriostatic activity throughout time, proving that biodegradable, non-toxic coatings can minimise microbial contamination and increase shelf life [126].

Amylose customises starch-gelatin composite films' barrier properties for various packaging purposes.   30% starch lowers water vapour permeability at 90% relative humidity (RH), but 20% high amylose and normal maize starches reduce oxygen permeability [126]. High-amylose starch increases film strength, whereas waxy maize starch (rich in amylopectin) increases flexibility, allowing film compositions to be optimised for specific purposes [126–128] High-amylose starch–gelatin films with B-type crystallinity have better mechanical qualities and barrier performance, making them suitable for food packaging that requires durability and eco-friendliness Click or tap here to enter text.

Table 4: Application of materials and its relevance

| Materials | Modifier or Filler | Key Properties | Relevance |
| --- | --- | --- | --- |
| WMS+PVA films | Cardanol oil/Sorbitol | Tensile strength, thermal stability, biodegradability, UV absorbance improved. | Shows that WMS may be used to make biodegradable packaging sheets with good mechanical and thermal properties [121] |
| Nanocellulose-reinforced native maize or starch sheets | Nanocellulose | Improved mechanical strength, barrier characteristics, water/oxygen resistance, and stability over pure starch films [129] | Reinforcement techniques like WMS+nanocellulose may provide high-performance WMS films with enhanced strength and durability. |
| Plain starch films (unmodified) | No or basic plasticisers | Low-cost and biodegradable, but weak mechanical strength, hydrophilicity, water sensitivity, and barrier characteristics [130]. | Indicates why WMS mixes or composites are needed and the baseline restrictions they must overcome. |
| ZnO nanoparticle-based starch nanocomposite films | ZnO NPs | Increased mechanical strength, UV-blocking, antimicrobial, durability, and packaging performance [131] | Shows how non-biopolymer fillers can improve performance; recommends a hybrid strategy: WMS + biodegradable fillers + inorganic additives for multifunctional packaging. |

The renewability, film-forming ability, and functionalisation potential of WMS-based films and composites make them promising biodegradable packaging. With suitable processing (pre-gelatinization, plasticization), WMS films can fulfil packaging requirements for tensile strength, thermal stability, and UV absorption. Biopolymer matrices reinforced with nanocellulose (typically starch or corn-based films) increase mechanical and barrier qualities, suggesting that WMS matrices might generate high-performance films with better durability and water sensitivity. Unmodified starch films violate current package mechanical and barrier standards due to brittleness, moisture absorption, and poor barrier performance. In starch-based films, inorganic nanoparticles like ZnO can provide multifunctional packaging with mechanical strength, antibacterial activity, and UV protection. WMS combined with biodegradable nano reinforcements or functional fillers can make packaging materials sustainable, functional, and competitive with petroleum-based plastics, solving environmental concerns while satisfying performance needs.

8.0 CONCLUSION

A adaptable and sustainable basis for self-healing polymer composites with better mechanical integrity, environmental stability, and functional performance is waxy maize starch.   Nanocrystal reinforcement, citric acid and Ca²⁺ cross-linking, antimicrobial compounds, and sophisticated microcapsule technologies enable WMS-based materials to self-repair microcracks and preserve protective barrier qualities for long-term usage   Recent research show WMS is a renewable alternative to petroleum-based systems because to improvements in healing efficiency, tensile strength, thermal stability, and biodegradability.   As sustainable materials become more popular, waxy maize starch-based self-healing composites might lead to circular, green, high-performance packaging and functional films for industry.

7.0 CHALLENGES AND FUTURE OUTLOOK

Despite encouraging developments in self-healing starch materials, numerous key constraints remain across techniques viz:

- Starch-Based Self-Healing Materials Limitations:   The microcapsule-based technology heals microcracks at 58.33% for enzyme-modified waxy maize starch (EWMS) and 44.65% for WMS, demonstrating inadequate repair even under ideal circumstances [17]. Dynamic imine networks improve mechanical recovery (87.5% tensile strength, 92.9% elongation at break) [11], both methods struggle with moisture sensitivity, with microcapsule sheets exhibiting transmission coefficients of 2.875-3.512 × 10⁻¹² g·cm/cm²·s·Pa [17] , even hydrophobic imine-crosslinked films need water resistance engineering to reach 109.2° [11] . In the intricate multi-step production of the microcapsule system, precision emulsification, high-speed dispersion (10,000 rpm), overnight solvent evaporation, and several centrifugation cycles provide scale-up issues [17], while the imine network requires 8-hour reaction periods at 50°C, 30 MPa heat-pressing conditions at 70°C, and careful amino-to-aldehyde ratio monitoring to preserve excellent characteristics [11]. These processing difficulties, specialised equipment, and precise environmental control hinder industrial-scale manufacture and practical use of self-healing starch materials.

- Starch-Based Hydrogel System Research Directions:  Three key areas of study should develop starch-based hydrogel technology.

- Hybridisation: Procedures might combine calcium-mediated ionic synergistic crosslinking [71–73] using natural starch reinforcement in double-network hydrogels [13], developing materials with high mechanical characteristics (>200 kPa tensile strength) and self-healing efficiency (>99%).

- Smart responsiveness: Is promising since current systems have self-healable ionic conductivity and variable rheology [13], which can possibly become pH, temperature, and electrically sensitive materials for soft robotics and wearable sensors.

- Scalability and processing optimisation:  Studies involving extrusion modification parameters [71] can be integrated using gelatinisation processes, hence, allowing industrial-scale production using dense microporous networks [71] that support gel excellence.  Alternatively, natural polysaccharides and metal ion combinations beyond Ca²⁺ may reveal synergistic crosslinking processes [71–73], while systematic investigations on long-term stability, biodegradability, and biocompatibility would help develop tissue engineering, medication delivery, and sustainable packaging materials from lab to market.

DISCLAIMER (ARTIFICIAL INTELLIGENCE)

Author(s) hereby declare that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc) and text-to-image generators have been used during the writing or editing of this manuscript.

References

1. 	Arum, C.T., Bbumba, S., Kigozi, M., Karume, I., Kato, M., Yikii, C.L., Kiganda, I.: Self-healing Building Materials for Enhanced Durability and Sustainability in Construction. Asian Journal of Chemical Sciences. 14, 25–36 (2024)

2. 	Engel, J.B., Ambrosi, A., Tessaro, I.C.: Development of biodegradable starch-based foams incorporated with grape stalks for food packaging. Carbohydr Polym. 225, 115234 (2019)

3. 	Jiang, T., Duan, Q., Zhu, J., Liu, H., Yu, L.: Starch-based biodegradable materials: Challenges and opportunities. Advanced Industrial and Engineering Polymer Research. 3, 8–18 (2020)

4. 	Nevoralová, M., Koutný, M., Ujčić, A., Horák, P., Kredatusová, J., Šerá, J., Růžek, L., Růžková, M., Krejčíková, S., Šlouf, M.: Controlled biodegradability of functionalized thermoplastic starch based materials. Polym Degrad Stab. 170, 108995 (2019)

5. 	Moad, G.: Chemical modification of starch by reactive extrusion. Prog Polym Sci. 36, 218–237 (2011)

6. 	Gao, J., Vasanthan, T., Hoover, R., Li, J.: Structural modification of waxy, regular, and high‐amylose maize and hulless barley starches on partial acid hydrolysis and their impact on physicochemical properties and chemical modification. Starch‐Stärke. 64, 313–325 (2012)

7. 	Stepto, R.F.T.: Thermoplastic starch. In: Macromolecular Symposia. pp. 163–168. Wiley Online Library (2009)

8. 	Abral, H., Atmajaya, A., Mahardika, M., Hafizulhaq, F., Handayani, D., Sapuan, S.M., Ilyas, R.A.: Effect of ultrasonication duration of polyvinyl alcohol (PVA) gel on characterizations of PVA film. Journal of Materials Research and Technology. 9, 2477–2486 (2020)

9. 	Angellier, H., Molina-Boisseau, S., Dufresne, A.: Mechanical properties of waxy maize starch nanocrystal reinforced natural rubber. Macromolecules. 38, 9161–9170 (2005)

10. 	Angellier, H., Molina-Boisseau, S., Dufresne, A.: Mechanical properties of waxy maize starch nanocrystal reinforced natural rubber. Macromolecules. 38, 9161–9170 (2005)

11. 	Zhang, X., Zhang, H., Zhou, G., Su, Z., Wang, X.: Flexible, thermal processable, self-healing, and fully bio-based starch plastics by constructing dynamic imine network. Green Energy & Environment. 9, 1610–1618 (2024)

12. 	Lu, K., Lan, X., Folkersma, R., Voet, V.S.D., Loos, K.: Borax Cross-Linked Acrylamide-Grafted Starch Self-Healing Hydrogels. Biomacromolecules. 25, 8026–8037 (2024)

13. 	Shang, X., Wang, Q., Li, J., Zhang, G., Zhang, J., Liu, P., Wang, L.: Double-network hydrogels with superior self-healing properties using starch reinforcing strategy. Carbohydr Polym. 257, 117626 (2021)

14. 	Lu, K., He, X., Burhani, D., Hu, J., Rudolf, P., Maniar, D., Folkersma, R., Voet, V.S.D., Loos, K.: Self-Healing, Remoldable, and Conductive Starch-Based Dual Reversible Cross-Linking Hydrogels for Strain Sensors. ACS Appl Mater Interfaces. (2025)

15. 	Chen, T., Chen, X., Lin, Z., Zhang, Y., Zhao, G., Xu, L., Peng, X., Wu, B.: Biodegradable, Stretchable, and Self‐Healing Starch‐Based Hydrogel with Intelligent Multi‐Bond Network Facilitated by MXene Nanosheets for Multifunctional Wearable Electronics. Advanced Materials. e12267 (2025)

16. 	Ke, T., Zhao, L., Fan, X., Gu, H.: Rapid self-healing, self-adhesive, anti-freezing, moisturizing, antibacterial and multi-stimuli-responsive PVA/starch/tea polyphenol-based composite conductive organohydrogel as flexible strain sensor. J Mater Sci Technol. 135, 199–212 (2023)

17. 	Guo, L., Yang, N., Gao, W., Tao, H., Cui, B., Liu, P., Zou, F., Lu, L., Fang, Y., Wu, Z.: Self-healing properties of retrograded starch films with enzyme-treated waxy maize starch as healing agent. Carbohydr Polym. 299, 120238 (2023)

18. 	Alabi, O.A., Ologbonjaye, K.I., Awosolu, O., Alalade, O.E.: Public and environmental health effects of plastic wastes disposal: a review. J Toxicol Risk Assess. 5, 1–13 (2019)

19. 	Gupta, K.K., Sharma, K.K., Chandra, H.: M icrococcus luteus strain CGK112 isolated from cow dung demonstrated efficient biofilm-forming ability and degradation potential toward high-density polyethylene (HDPE). Arch Microbiol. 204, 402 (2022)

20. 	Queiroz, A.U.B., Collares-Queiroz, F.P.: Innovation and industrial trends in bioplastics. Journal of Macromolecular Science®, Part C: Polymer Reviews. 49, 65–78 (2009)

21. 	Luckachan, G.E., Pillai, C.K.S.: Biodegradable polymers-a review on recent trends and emerging perspectives. J Polym Environ. 19, 637–676 (2011)

22. 	Li, J., Dou, Y., Yang, J., Yin, Y., Zhang, H., Yao, F., Wang, H., Yao, K.: Surface characterization and biocompatibility of micro-and nano-hydroxyapatite/chitosan-gelatin network films. Materials Science and Engineering: C. 29, 1207–1215 (2009)

23. 	Kadam, S.U., Pankaj, S.K., Tiwari, B.K., Cullen, P.J., O’Donnell, C.P.: Development of biopolymer-based gelatin and casein films incorporating brown seaweed Ascophyllum nodosum extract. Food Packag Shelf Life. 6, 68–74 (2015)

24. 	Cano, A., Jiménez, A., Cháfer, M., Gónzalez, C., Chiralt, A.: Effect of amylose: amylopectin ratio and rice bran addition on starch films properties. Carbohydr Polym. 111, 543–555 (2014)

25. 	Zhang, Y., Thompson, M., Liu, Q.: The effect of pea fiber and potato pulp on thermal property, surface tension, and hydrophilicity of extruded starch thermoplastics. Carbohydr Polym. 86, 700–707 (2011)

26. 	Vilaplana, F., Hasjim, J., Gilbert, R.G.: Amylose content in starches: Toward optimal definition and validating experimental methods. Carbohydr Polym. 88, 103–111 (2012)

27. 	Li, M., Liu, P., Zou, W., Yu, L., Xie, F., Pu, H., Liu, H., Chen, L.: Extrusion processing and characterization of edible starch films with different amylose contents. J Food Eng. 106, 95–101 (2011)

28. 	Romero-Bastida, C.A., Bello-Pérez, L.A., Velazquez, G., Alvarez-Ramirez, J.: Effect of the addition order and amylose content on mechanical, barrier and structural properties of films made with starch and montmorillonite. Carbohydr Polym. 127, 195–201 (2015)

29. 	Vandeputte, G.E., Vermeylen, R., Geeroms, J., Delcour, J.A.: Rice starches. III. Structural aspects provide insight in amylopectin retrogradation properties and gel texture. J Cereal Sci. 38, 61–68 (2003)

30. 	Bodini, R.B., Sobral, P.J. do A., Fávaro-Trindade, C.S., Carvalho, R.A. de: Properties of gelatin-based films with added ethanol–propolis extract. LWT-Food Science and Technology. 51, 104–110 (2013)

31. 	Sun, Q., Sun, C., Xiong, L.: Mechanical, barrier and morphological properties of pea starch and peanut protein isolate blend films. Carbohydr Polym. 98, 630–637 (2013)

32. 	Jiamjariyatam, R., Kongpensook, V., Pradipasena, P.: Effects of amylose content, cooling rate and aging time on properties and characteristics of rice starch gels and puffed products. J Cereal Sci. 61, 16–25 (2015)

33. 	Stading, M., Hermansson, A.-M., Gatenholm, P.: Structure, mechanical and barrier properties of amylose and amylopectin films. Carbohydr Polym. 36, 217–224 (1998)

34. 	Sabetzadeh, M., Bagheri, R., Masoomi, M.: Study on ternary low density polyethylene/linear low density polyethylene/thermoplastic starch blend films. Carbohydr Polym. 119, 126–133 (2015)

35. 	Kaseem, M., Hamad, K., Deri, F.: Rheological and mechanical properties of polypropylene/thermoplastic starch blend. Polymer bulletin. 68, 1079–1091 (2012)

36. 	Noivoil, N., Yoksan, R.: Compatibility improvement of poly (lactic acid)/thermoplastic starch blown films using acetylated starch. J Appl Polym Sci. 138, 49675 (2021)

37. 	Temesgen, S., Rennert, M., Tesfaye, T., Nase, M.: Review on spinning of biopolymer fibers from starch. Polymers (Basel). 13, 1121 (2021)

38. 	Abral, H., Ariksa, J., Mahardika, M., Handayani, D., Aminah, I., Sandrawati, N., Sapuan, S.M., Ilyas, R.A.: Highly transparent and antimicrobial PVA based bionanocomposites reinforced by ginger nanofiber. Polym Test. 81, 106186 (2020)

39. 	Ge, C., Lansing, B., Lewis, C.L.: Thermoplastic starch and poly (vinyl alcohol) blends centered barrier film for food packaging applications. Food Packag Shelf Life. 27, 100610 (2021)

40. 	Lu, K., Lan, X., Folkersma, R., Voet, V.S.D., Loos, K.: Borax Cross-Linked Acrylamide-Grafted Starch Self-Healing Hydrogels. Biomacromolecules. 25, 8026–8037 (2024). https://doi.org/10.1021/acs.biomac.4c01287

41. 	Kim, J.R., Netravali, A.N.: Self‐healing properties of protein resin with soy protein isolate‐loaded poly (D, L‐lactide‐co‐glycolide) microcapsules. Adv Funct Mater. 26, 4786–4796 (2016)

42. 	Gandini, A.: Polymers from renewable resources: a challenge for the future of macromolecular materials. Macromolecules. 41, 9491–9504 (2008)

43. 	Kim, J.R., Netravali, A.N.: Self-healing starch-based ‘green’thermoset resin. Polymer (Guildf). 117, 150–159 (2017)

44. 	Kim, J.R., Netravali, A.N.: Self-healing green composites based on soy protein and microfibrillated cellulose. Compos Sci Technol. 143, 22–30 (2017)

45. 	Kim, J.T., Netravali, A.N.: Mechanical, thermal, and interfacial properties of green composites with ramie fiber and soy resins. J Agric Food Chem. 58, 5400–5407 (2010)

46. 	Gross, R.A., Kalra, B.: Biodegradable polymers for the environment. Science (1979). 297, 803–807 (2002)

47. 	Lin, T., Zhang, X., Tang, Z., Guo, B.: Renewable conjugated acids as curatives for high-performance rubber/silica composites. Green Chemistry. 17, 3301–3305 (2015)

48. 	Venkatanarasimhan, S., Raghavachari, D.: Epoxidized natural rubber–magnetite nanocomposites for oil spill recovery. J Mater Chem A Mater. 1, 868–876 (2013)

49. 	Matsuda, S., Iwata, H., Se, N., Ikada, Y.: Bioadhesion of gelatin films crosslinked with glutaraldehyde. Journal of Biomedical Materials Research: An Official Journal of The Society for Biomaterials, The Japanese Society for Biomaterials, and The Australian Society for Biomaterials. 45, 20–27 (1999)

50. 	Wu, J., Muir, A.D.: Comparative structural, emulsifying, and biological properties of 2 major canola proteins, cruciferin and napin. J Food Sci. 73, C210–C216 (2008)

51. 	Liu, Z., Luo, Y., Bai, H., Zhang, Q., Fu, Q.: Remarkably enhanced impact toughness and heat resistance of poly (L-lactide)/thermoplastic polyurethane blends by constructing stereocomplex crystallites in the matrix. ACS Sustain Chem Eng. 4, 111–120 (2016)

52. 	Kim, J.R., Netravali, A.N.: Self-healing starch-based ‘green’thermoset resin. Polymer (Guildf). 117, 150–159 (2017)

53. 	Samadzadeh, M., Boura, S.H., Peikari, M., Kasiriha, S.M., Ashrafi, A.: A review on self-healing coatings based on micro/nanocapsules. Prog Org Coat. 68, 159–164 (2010)

54. 	White, S.R., Sottos, N.R., Geubelle, P.H., Moore, J.S., Kessler, M.R., Sriram, S.R., Brown, E.N., Viswanathan, S.: Autonomic healing of polymer composites. Nature. 409, 794–797 (2001)

55. 	Lanzara, G., Yoon, Y., Liu, H., Peng, S., Lee, W.I.: Carbon nanotube reservoirs for self-healing materials. Nanotechnology. 20, 335704 (2009)

56. 	Wu, D.Y., Meure, S., Solomon, D.: Self-healing polymeric materials: A review of recent developments. Prog Polym Sci. 33, 479–522 (2008)

57. 	Wertz, J.T., Mauldin, T.C., Boday, D.J.: Polylactic acid with improved heat deflection temperatures and self-healing properties for durable goods applications. ACS Appl Mater Interfaces. 6, 18511–18516 (2014)

58. 	Burfield, D.R., Lim, K.-L., Law, K.-S., Ng, S.: Analysis of epoxidized natural rubber. A comparative study of dsc, nmr, elemental analysis and direct titration methods. Polymer (Guildf). 25, 995–998 (1984)

59. 	Wei, Z., Yang, J.H., Liu, Z.Q., Xu, F., Zhou, J.X., Zrínyi, M., Osada, Y., Chen, Y.M.: Novel biocompatible polysaccharide‐based self‐healing hydrogel. Adv Funct Mater. 25, 1352–1359 (2015)

60. 	Ogawa, Y., OKADA, H., YAMAMOTO, Y., SHIMAMOTO, T.: In vivo release profiles of leuprolide acetate from microcapsules prepared with polylactic acids or copoly (lactic/glycolic) acids and in vivo degradation of these polymers. Chem Pharm Bull (Tokyo). 36, 2576–2581 (1988)

61. 	Zdanowicz, M., Johansson, C.: Mechanical and barrier properties of starch-based films plasticized with two-or three component deep eutectic solvents. Carbohydr Polym. 151, 103–112 (2016)

62. 	Fabra, M.J., López-Rubio, A., Cabedo, L., Lagaron, J.M.: Tailoring barrier properties of thermoplastic corn starch-based films (TPCS) by means of a multilayer design. J Colloid Interface Sci. 483, 84–92 (2016)

63. 	Maran, J.P., Sivakumar, V., Thirugnanasambandham, K., Kandasamy, S.: Modeling and analysis of film composition on mechanical properties of maize starch based edible films. Int J Biol Macromol. 62, 565–573 (2013)

64. 	Da Silva, J.B.A., Pereira, F. V, Druzian, J.I.: Cassava starch‐based films plasticized with sucrose and inverted sugar and reinforced with cellulose nanocrystals. J Food Sci. 77, N14–N19 (2012)

65. 	Fazeli, M., Keley, M., Biazar, E.: Preparation and characterization of starch-based composite films reinforced by cellulose nanofibers. Int J Biol Macromol. 116, 272–280 (2018)

66. 	Angellier, H., Molina-Boisseau, S., Dole, P., Dufresne, A.: Thermoplastic starch− waxy maize starch nanocrystals nanocomposites. Biomacromolecules. 7, 531–539 (2006)

67. 	Maran, J.P., Sivakumar, V., Sridhar, R., Thirugnanasambandham, K.: Development of model for barrier and optical properties of tapioca starch based edible films. Carbohydr Polym. 92, 1335–1347 (2013)

68. 	Wang, Y., Yuan, C., Liu, Y., Xu, D., Cui, B.: The influence of a hydroxypropyl-beta-cyclodextrin composite on the gelation of kappa-carrageenan. Food Hydrocoll. 90, 276–284 (2019)

69. 	Saltmarsh, M.: Recent trends in the use of food additives in the United Kingdom. J Sci Food Agric. 95, 649–652 (2015)

70. 	Fang, Y., Fu, J., Tao, C., Liu, P., Cui, B.: Mechanical properties and antibacterial activities of novel starch-based composite films incorporated with salicylic acid. Int J Biol Macromol. 155, 1350–1358 (2020). https://doi.org/10.1016/j.ijbiomac.2019.11.110

71. 	Wei, W., Wu, M., Zhang, T., Zhang, X., Ren, W., He, T.: Enhancement of Starch Gel Properties Using Ionic Synergistic Multiple Crosslinking Extrusion Modification. Foods. 13, 24 (2023)

72. 	Sornsumdaeng, K., Seeharaj, P., Prachayawarakorn, J.: Property improvement of biodegradable citric acid-crosslinked rice starch films by calcium oxide. Int J Biol Macromol. 193, 748–757 (2021)

73. 	Wurm, F., Rietzler, B., Pham, T., Bechtold, T.: Multivalent ions as reactive crosslinkers for biopolymers—a review. Molecules. 25, 1840 (2020)

74. 	Ning, D., Songfeng, E., Ma, Q., Zhao, R., Jia, F., Lu, Z.: Strong, tough and degradable cellulose nanofibers-based composite film by the dual crosslinking of polydopamine and iron ions. Compos Sci Technol. 220, 109299 (2022)

75. 	Su, T., Wu, L., Zuo, G., Pan, X., Shi, M., Zhang, C., Qi, X., Dong, W.: Incorporation of dumbbell-shaped and Y-shaped cross-linkers in adjustable pullulan/polydopamine hydrogels for selective adsorption of cationic dyes. Environ Res. 182, 109010 (2020)

76. 	Camani, P.H., Gonçalo, M.G.M., Barbosa, R.F.S., Rosa, D.S.: Comprehensive insight of crosslinking agent concentration influence on starch‐based aerogels porous structure. J Appl Polym Sci. 138, 50863 (2021)

77. 	da Silva Fernandes, R., Tanaka, F.N., de Moura, M.R., Aouada, F.A.: Development of alginate/starch-based hydrogels crosslinked with different ions: Hydrophilic, kinetic and spectroscopic properties. Mater Today Commun. 21, 100636 (2019)

78. 	Sabadini, R.C., Fernandes, M., de Zea Bermudez, V., Pawlicka, A., Silva, M.M.: Eco‐friendly superabsorbent hydrogels based on starch, gellan gum, citric acid, and nanoclays for soil humidity control. J Appl Polym Sci. 139, e52998 (2022)

79. 	Qin, Y., Zhang, S., Yu, J., Yang, J., Xiong, L., Sun, Q.: Effects of chitin nano-whiskers on the antibacterial and physicochemical properties of maize starch films. Carbohydr Polym. 147, 372–378 (2016)

80. 	Ortega-Toro, R., Collazo-Bigliardi, S., Roselló, J., Santamarina, P., Chiralt, A.: Antifungal starch-based edible films containing Aloe vera. Food Hydrocoll. 72, 1–10 (2017)

81. 	Nouri, L., Nafchi, A.M.: Antibacterial, mechanical, and barrier properties of sago starch film incorporated with betel leaves extract. Int J Biol Macromol. 66, 254–259 (2014)

82. 	Qiu, C., Qin, Y., Zhang, S., Xiong, L., Sun, Q.: A comparative study of size-controlled worm-like amylopectin nanoparticles and spherical amylose nanoparticles: Their characteristics and the adsorption properties of polyphenols. Food Chem. 213, 579–587 (2016)

83. 	da Rocha Neto, A.C., Maraschin, M., Di Piero, R.M.: Antifungal activity of salicylic acid against Penicillium expansum and its possible mechanisms of action. Int J Food Microbiol. 215, 64–70 (2015)

84. 	Panahirad, S., Zaare‐Nahandi, F., Safaralizadeh, R., Alizadeh‐Salteh, S.: Postharvest Control of R hizopus stolonifer in Peach (P runus persica L. B atsch) Fruits Using Salicylic Acid. J Food Saf. 32, 502–507 (2012)

85. 	Daw, B.D., Zhang, L.H., Wang, Z.Z.: Salicylic acid enhances antifungal resistance to Magnaporthe grisea in rice plants. Australasian Plant Pathology. 37, 637–644 (2008)

86. 	Gillgren, T., Faye, M.-V., Stading, M.: Mechanical and barrier properties of films from millet protein pennisetin. Food Biophys. 6, 474–480 (2011)

87. 	Martínez-Ortiz, M.A., Vargas-Torres, A., Román-Gutiérrez, A.D., Chavarría-Hernández, N., Zamudio-Flores, P.B., Meza-Nieto, M., Palma-Rodríguez, H.M.: Partial characterization of chayotextle starch-based films added with ascorbic acid encapsulated in resistant starch. Int J Biol Macromol. 98, 341–347 (2017)

88. 	Liu, P., Wang, R., Kang, X., Cui, B., Yu, B.: Effects of ultrasonic treatment on amylose-lipid complex formation and properties of sweet potato starch-based films. Ultrason Sonochem. 44, 215–222 (2018)

89. 	Qiao, D., Li, S., Yu, L., Zhang, B., Simon, G., Jiang, F.: Effect of alkanol surface grafting on the hydrophobicity of starch-based films. Int J Biol Macromol. 112, 761–766 (2018)

90. 	Issa, A., Ibrahim, S.A., Tahergorabi, R.: Impact of sweet potato starch-based nanocomposite films activated with thyme essential oil on the shelf-life of baby spinach leaves. Foods. 6, 43 (2017)

91. 	Liu, S., Li, X., Chen, L., Li, L., Li, B., Zhu, J.: Tunable d-limonene permeability in starch-based nanocomposite films reinforced by cellulose nanocrystals. J Agric Food Chem. 66, 979–987 (2018)

92. 	Dai, L., Qiu, C., Xiong, L., Sun, Q.: Characterisation of corn starch-based films reinforced with taro starch nanoparticles. Food Chem. 174, 82–88 (2015)

93. 	Ai, J., Li, K., Li, J., Yu, F., Ma, J.: Super flexible, fatigue resistant, self-healing PVA/xylan/borax hydrogel with dual-crosslinked network. Int J Biol Macromol. 172, 66–73 (2021)

94. 	Li, M., Han, X., Fan, Z., Zhang, Y., Li, Q., Xie, G.: Autonomous ultrafast-self-healing hydrogel for application in multiple environments. Colloids Surf A Physicochem Eng Asp. 631, 127669 (2021)

95. 	Long, T., Li, Y., Fang, X., Sun, J.: Salt‐mediated polyampholyte hydrogels with high mechanical strength, excellent self‐healing property, and satisfactory electrical conductivity. Adv Funct Mater. 28, 1804416 (2018)

96. 	Nakahata, M., Takashima, Y., Yamaguchi, H., Harada, A.: Redox-responsive self-healing materials formed from host–guest polymers. Nat Commun. 2, 511 (2011)

97. 	Chao, A., Negulescu, I., Zhang, D.: Dynamic covalent polymer networks based on degenerative imine bond exchange: tuning the malleability and self-healing properties by solvent. Macromolecules. 49, 6277–6284 (2016)

98. 	Chen, Y., Guan, Z.: Multivalent hydrogen bonding block copolymers self-assemble into strong and tough self-healing materials. Chemical Communications. 50, 10868–10870 (2014)

99. 	Huang, S., Shuyi, S., Gan, H., Linjun, W., Lin, C., Danyuan, X., Zhou, H., Lin, X., Qin, Y.: Facile fabrication and characterization of highly stretchable lignin-based hydroxyethyl cellulose self-healing hydrogel. Carbohydr Polym. 223, 115080 (2019)

100. 	Shao, C., Wang, M., Chang, H., Xu, F., Yang, J.: A self-healing cellulose nanocrystal-poly (ethylene glycol) nanocomposite hydrogel via Diels–Alder click reaction. ACS Sustain Chem Eng. 5, 6167–6174 (2017)

101. 	Pepels, M., Filot, I., Klumperman, B., Goossens, H.: Self-healing systems based on disulfide–thiol exchange reactions. Polym Chem. 4, 4955–4965 (2013)

102. 	Cheng, H., Fan, Z., Wang, Z., Guo, Z., Jiang, J., Xie, Y.: Highly stretchable, fast self-healing nanocellulose hydrogel combining borate ester bonds and acylhydrazone bonds. Int J Biol Macromol. 245, 125471 (2023)

103. 	Rumon, M.M.H., Akib, A.A., Sultana, F., Moniruzzaman, M., Niloy, M.S., Shakil, M.S., Roy, C.K.: Self-healing hydrogels: Development, biomedical applications, and challenges. Polymers (Basel). 14, 4539 (2022)

104. 	Ren, Z., Ke, T., Ling, Q., Zhao, L., Gu, H.: Rapid self-healing and self-adhesive chitosan-based hydrogels by host-guest interaction and dynamic covalent bond as flexible sensor. Carbohydr Polym. 273, 118533 (2021)

105. 	Seidi, F., Jin, Y., Han, J., Saeb, M.R., Akbari, A., Hosseini, S.H., Shabanian, M., Xiao, H.: Self‐healing polyol/borax hydrogels: fabrications, properties and applications. The Chemical Record. 20, 1142–1162 (2020)

106. 	Mate, C.J., Mishra, S.: Synthesis of borax cross-linked Jhingan gum hydrogel for remediation of Remazol Brilliant Blue R (RBBR) dye from water: adsorption isotherm, kinetic, thermodynamic and biodegradation studies. Int J Biol Macromol. 151, 677–690 (2020)

107. 	Dai, L., Nadeau, B., An, X., Cheng, D., Long, Z., Ni, Y.: Silver nanoparticles-containing dual-function hydrogels based on a guar gum-sodium borohydride system. Sci Rep. 6, 36497 (2016)

108. 	Koga, K., Takada, A., Nemoto, N.: Dynamic light scattering and dynamic viscoelasticity of poly (vinyl alcohol) in aqueous borax solutions. 5. Temperature effects. Macromolecules. 32, 8872–8879 (1999)

109. 	Sánchez, T., Salcedo, E., Ceballos, H., Dufour, D., Mafla, G., Morante, N., Calle, F., Pérez, J.C., Debouck, D., Jaramillo, G.: Screening of starch quality traits in cassava (Manihot esculenta Crantz). Starch‐Stärke. 61, 12–19 (2009)

110. 	Taylor, D.L., In Het Panhuis, M.: Self‐healing hydrogels. Advanced Materials. 28, 9060–9093 (2016)

111. 	Zhang, R., Ruan, H., Zhou, T., Fu, Q., Peng, H., Zhu, X., Yao, Y.: High-performance poly (acrylic acid) hydrogels formed with a block copolymer crosslinker containing amino-acid derivatives. Soft Matter. 15, 7381–7389 (2019)

112. 	Xu, D., Huang, J., Zhao, D., Ding, B., Zhang, L., Cai, J.: High‐flexibility, high‐toughness double‐cross‐linked chitin hydrogels by sequential chemical and physical cross‐linkings. Advanced Materials. 28, 5844–5849 (2016)

113. 	Lu, K., Lan, X., Folkersma, R., Voet, V.S.D., Loos, K.: Borax Cross-Linked Acrylamide-Grafted Starch Self-Healing Hydrogels. Biomacromolecules. 25, 8026–8037 (2024)

114. 	Chen, X., Ji, N., Li, F., Qin, Y., Wang, Y., Xiong, L., Sun, Q.: Dual cross-linked starch–borax double network hydrogels with tough and self-healing properties. Foods. 11, 1315 (2022)

115. 	Ramesh, M., Kumar, L.R., Khan, A., Asiri, A.M.: Self-healing polymer composites and its chemistry. In: Self-healing composite materials. pp. 415–427. Elsevier (2020)

116. 	Scheiner, M., Dickens, T.J., Okoli, O.: Progress towards self-healing polymers for composite structural applications. Polymer (Guildf). 83, 260–282 (2016)

117. 	Thakur, V.K., Kessler, M.R.: Self-healing polymer nanocomposite materials: A review. Polymer (Guildf). 69, 369–383 (2015)

118. 	Lu, K., Lan, X., Folkersma, R., Voet, V.S.D., Loos, K.: Borax Cross-Linked Acrylamide-Grafted Starch Self-Healing Hydrogels. Biomacromolecules. 25, 8026–8037 (2024)

119. 	Souzandeh, H., Netravali, A.N.: Self-healing of ‘green’thermoset zein resins with irregular shaped waxy maize starch-based/poly (D, L-lactic-co-glycolic acid) microcapsules. Compos Sci Technol. 183, 107831 (2019)

120. 	Liu, C., Li, K., Li, X., Zhang, M., Li, J.: Formation and structural evolution of starch nanocrystals from waxy maize starch and waxy potato starch. Int J Biol Macromol. 180, 625–632 (2021)

121. 	Yahia, R., Owda, M.E., Abou-Zeid, R.E., Abdelhai, F., El-Gamil, H.Y., Abdo, A.M., Ali, A.A.: Biodegradable, UV absorber and thermal stable bioplastic films from waxy corn starch/polyvinyl alcohol blends. Biomass Convers Biorefin. 14, 27989–28006 (2024)

122. 	Sabapathy, P.C., Parthiban, A., Bhusal, C.K., Singh, S., Sehgal, R., Qi, X.: Recent improvements in starch films with cellulose and its derivatives–A review. J Taiwan Inst Chem Eng. 105920 (2024)

123. 	Guimarães Jr, M., Botaro, V.R., Novack, K.M., Teixeira, F.G., Tonoli, G.H.D.: Starch/PVA-based nanocomposites reinforced with bamboo nanofibrils. Ind Crops Prod. 70, 72–83 (2015)

124. 	Salleh, M.S.N., Nor, N.N.M., Mohd, N., Draman, S.F.S.: Water resistance and thermal properties of polyvinyl alcohol-starch fiber blend film. In: AIP conference proceedings. p. 020045. AIP Publishing LLC (2017)

125. 	Turco, R., Ortega-Toro, R., Tesser, R., Mallardo, S., Collazo-Bigliardi, S., Chiralt Boix, A., Malinconico, M., Rippa, M., Di Serio, M., Santagata, G.: Poly (lactic acid)/thermoplastic starch films: Effect of cardoon seed epoxidized oil on their chemicophysical, mechanical, and barrier properties. Coatings. 9, 574 (2019)

126. 	Wang, K., Wang, W., Ye, R., Xiao, J., Liu, Y., Ding, J., Zhang, S., Liu, A.: Mechanical and barrier properties of maize starch–gelatin composite films: effects of amylose content. J Sci Food Agric. 97, 3613–3622 (2017)

127. 	Acosta, S., Jiménez, A., Cháfer, M., González-Martínez, C., Chiralt, A.: Physical properties and stability of starch-gelatin based films as affected by the addition of esters of fatty acids. Food Hydrocoll. 49, 135–143 (2015)

128. 	Almasi, H., Ghanbarzadeh, B., Entezami, A.A.: Physicochemical properties of starch–CMC–nanoclay biodegradable films. Int J Biol Macromol. 46, 1–5 (2010)

129. 	Patil, S., Bharimalla, A.K., Nadanathangam, V., Dhakane-Lad, J., Mahapatra, A., Jagajanantha, P., Saxena, S.: Nanocellulose reinforced corn starch-based biocomposite films: Composite optimization, characterization and storage studies. Food Packag Shelf Life. 33, 100860 (2022)

130. 	Surendren, A., Mohanty, A.K., Liu, Q., Misra, M.: A review of biodegradable thermoplastic starches, their blends and composites: recent developments and opportunities for single-use plastic packaging alternatives. Green Chemistry. 24, 8606–8636 (2022)

131. 	Dhiman, S., Kumari, A., Kumari, S., Sharma, R.: Advanced biodegradable starch-based nanocomposite films incorporating zinc oxide nanoparticles: Synthesis, characterization, and efficacy in antibacterial food packaging applications. J Environ Chem Eng. 13, 116296 (2025)

Click or tap here to enter text.