### Effect of adsorbents dosage, contact time, initial concentration, Temperature and pH,On the percentage removal of NO3-, PO4-3, Cu2+, Pb2+ and Cd2+ (adsorbates) onto Mukurweini’s kaolinite and alkali modified Kaolinite

### ABSTRACT

Access to clean and safe water for domestic and industrial use remains a major challenge for developing countries in the Third World. The available fresh water resources are distributed unevenly across the country, with the available sources affected by heavy pollution from sources such as raw sewage, domestic and industrial waste, agricultural waste, and emerging pollutants such as plastic, which contribute significantly to the limited accessibility of clean water in Kenya. These studies examined the potential application of clay-derived zeolites derived from clay material (kaolinite) obtained from Mukurweini in Nyeri County to remedy water contaminated with agricultural waste. To achieve optimum removal of pollutants in wastewater, batch adsorption studies were carried out to determine the optimum operating conditions, i.e., contact time, pH, and calcination temperature. The optimum calcination temperature was determined at t = 550–900 °C, equilibrium contact time of 30 minutes, pH = 7, and temperature t = 25 °C. At these optimum conditions, the overall percentage removal of NO3-, PO4-3, Cu2+, Pb2+ and Cd2+ (adsorbates) was calculated at 99.2% for solutions of concentration c = 100 ppm for all ions. The results show that the pH of the solution uniquely affected the adsorption capacities of the five adsorbed substances.

Keywords: Adsorption, Zeolites, Calcination, Emerging pollutants, modified kaolinite, Leaching

# INTRODUCTION

Water is polluted when undesired substances find their ways to it. Water has several properties such as being an excellent solvent and can dissolve several substances including toxic, substances that are harmful to human health[1]. Water pollution transpires in two ways. By direct contact of the pollutant with the water body such as the direct pouring of industrial wastewater into rivers or any water body, leakage of wastewater pipes, among others and by indirect and slowly contact of the pollutant with the water body such as leaching of agrochemicals that include fertilizers, pesticides into underground water, and malfunctioning of the septic tank [2].

Domestic and industrial sources largely contribute to water pollution. They include leakage of toxic substances such as radioactive elements, concentrated acids, and organic substances from wastewater pipes. Leaching of fertilizers used for home gardening. Inadequate functioning of the septic tank. Inappropriate disposal of waste from industrial to the general household activities.

Adsorption studies are carried in order to gain a better understanding of the interactions between molecules and surfaces. Adsorption is the process in which molecules of a material are attracted to and remain on the surface of a solid or liquid [3]. Through these studies, the ability to analyze the surface properties of materials, such as surface area, pore size, and porosity, which can be used to create new materials and improve existing ones, as well as to develop more efficient separation and purification processes.

Population growth has enormously contributed to the utilization of chemical fertilizers, which has indirectly contributed to water pollution[4]. Although chemical fertilizers contribute to water and air pollution, the usage of chemical fertilizer is an important part of agriculture activity. The maximum productivity of a land is guaranteed by the presence of sufficient nutrients in the soil but continuous mining of nutrients from soil by crops demands for the use of fertilizers to achieve the desired yields[5]. The drastic population growth in the past few decades has increased the demand for agricultural production and hence the need to increase the crop yield which has resulted in an overuse of chemical fertilizers.

Nitrate supplies nitrogen, which is an essential component for plant growth, and a major contributor for the production of amino acids used to synthesize proteins. Proteins are necessary for the wholesome growth and development of plants. They contribute to the phototropism regulation of the plant, which is an adjustment to light, and darkness; and generate energy from some chemical reactions that enable membrane transportation and the formation of the intracellular structure[6]. Therefore, nitrate deficiency affects plants growth considerably. It is noteworthy that nitrate is not found in fertilizer in a simple form; they are always combined with other elements such as ammonium nitrate or sometimes combines with some other essential metal for plant development such as calcium (calcium ammonium nitrate). Most of the time the ammonium nitrate is oxidized leading to the separation of ammonia and nitrate. Nitrate can be consumed directly from unwashed vegetables or through drinking water[7].

The nitrate accumulated on the soil through leaching pollutes the underground water and surface water by surface run-off. Nitrate intake has many implications for human health such as causing methemoglobinemia (blue baby syndrome) which is a haemoglobin disorder resulting from oxidation of haemoglobin. The oxidized haemoglobin became methemoglobin, which interferes with adequate distribution of oxygen in the blood to other body tissues[8].

Excess phosphate in a water body is always noticeable by eutrophication which occurs when a water body is excessively rich in nutrients especially phosphate[9]. The population growth, climate change and economic development contribute to increased demand for freshwater and therefore mitigation measures have to be taken to deal with eutrophication, which is a threat to water quality[9]. Eutrophication limits economic activities such as fishing, recreational use of water, as well as limiting accessibility to safe drinking water, among others. The decay of dead algae leads to accumulation of organic matter in the water body which results in the depletion of dissolved oxygen and subsequently, death of aquatic life[10]. Algae also produce some toxins, which are harmful to animal and human health, and can lead to several diseases such as neurotoxicity, liver damage, and eye and skin irritation among others[11].

Copper is one of the essential micronutrients that required for plant growth. It plays a significant role in photosynthesis and its deficiency is always detected by the colour change on the leaves and can lead to a considerable reduction of the crop yield [12]. It is mostly found in herbicides and sometimes in fertilizers. It is also an essential element for human health required in the formation of the red blood cells. Excess intake of copper however, is very harmful to human body as it may cause deadly diseases. It targets some specific body systems such as cardiovascular system by disrupting the red blood leading to the release of hemoglobin into the bloodstream, abnormally known as hemolysis. Accumulation of copper is also manifested in gastrointestinal system by nausea and vomiting. Its toxicity is mostly felt in the hepatic system where the high concentration damages the liver. High intake of copper also affects central nervous system and renal system leading to kidney failure[13].

Lead easily contaminates underground water through leaching and this has been witnessed in many sub-Saharans Africa countries. Lead intake mostly affects children neurological system by reduction the child’s IQ or attention span and some of these damages are irreversible. Lead can also affect an unborn child via the mother blood by either damaging the neurological system or by causing a miscarriage[14]. Additionally, it has an impact on the cardiovascular, renal, and reproductive systems, causing infertility for both male and female[15].

Cadmium is considered as a non-essential element for plant growth[16] Cadmium is present in fertilizer especially in phosphate fertilizers because of the presence of large amounts of cadmium in the phosphate rock[17]. The accumulation of cadmium in the soil and underground water is related to excessive utilization of chemical fertilizers. Excess cadmium affects plant development, pollute the environment and affect human health. Cadmium affects human health by damaging or preventing proper functioning of body organs.

Like arsenic, cadmium affects renal system manifested through nephropathy, which is the damage of the kidney blood vessel, preventing proper functioning of the kidney a dysfunction that might lead to kidney failure[18]. It affects skeleton system where cadmium interacts with bone cells reducing the bone mineralization and preventing the production of collagen. This leads to osteoporosis, a disease in which the bone becomes weak and susceptible to fracture[19].

# METHODS AND MATERIALS

The materials were collected from Nyeri County in Mukurweini, then dried in an oven at 80°C for 18 hours and finely ground using a motor and pestle. A part of this sample was then taken to a muffle furnace, where it was heated at 700°C for two hours. After this, it was hydrothermally treated with 8M of NaOH in a pressure cooker at 120°C for three hours. Finally, it was put back into the muffle furnace for two hours at 650°C. A batch adsorption study was conducted using two adsorbents, kaolinite and alkali-modified kaolinite, in order to determine the adsorption isotherm, adsorption kinetics, and adsorption thermodynamics.

The study was done using seven different adsorbents from different sampling points (S1, S2, S3, S4, S5, S6, and S7) and five different adsorbates (Nitrate, Phosphate, lead, Cadmium and Copper). Nitrate and Phosphate adsorption study was done using UV-VIS Spectrometer and Lead, Copper and Cadmium using AAS. The following parameters were analyzed: effect of dosage, effect contact time, effect of concentration, effect of pH, effect of temperature, adsorption isotherms, and adsorption kinetics and adsorption thermodynamics. It was observed that the adsorbents S1, S2, S3, S4, S5 and S6 had similar behavior throughout the adsorption study.

The batch adsorption study was carried out and the sample solutions analyzed alongside standard solutions using an AA-6300 SHIMADZU Atomic Absorption Spectrophotometer and the following procedure: The computer connected to the AAS was first turned on, as different parameters were set. The ASS lamp was setting based on the metal being analyzed (copper, lead and cadmium).  After that, the compressed air and acetylene cylinders valves were opened and the flame was ignited. Using the University of Nairobi laboratory standards, the calibration curve was set. Different prepared samples were then injected into the flame and their absorbance were recorded.

# Results and discussion

## Effect of dosage

The effect of dosage was conducted with an initial concentration of 10ppm, for 30minutes with a temperature of 298 K and a pH of 7.  The ranges of the adsorbents were within 0.1g to 0.020g for nitrate and phosphate; and 0.5g to 0.05g for cooper lead and cadmium.

Dosage is an essential factor in determining the number of sorption sites. From figure 1 to figure 14, the percentage removal of the adsorbate increased as the adsorbent dosage increased and declined as the adsorbent dosage decreased. This observation was similar to many other adsorption studies[20 & 21]. Therefore, more adsorbent means more sorption site, implying the presence more unbalance energy on the surface ready for intermolecular reactions[3].  The exception with this study was the removal of phosphate using kaolinite (S7). The adsorbent S7 was not able to remove phosphate. This is similar to the study done by[22] who found out that commercial kaolinite was not able to adsorb phosphate. Abosede et al.,[23] also concluded that adsorption of phosphate by kaolinite was not possible unless in an acidic medium.

Figure 1 Effect of adsorbents dosage on the percentage removal of NO3-

Figure 2 Effect of adsorbents dosage on the percentage removal of PO43-

Figure 3 Effect of adsorbents dosage on the percentage removal of Pb2+

Figure 4 Effect of adsorbents dosage on the percentage removal of Cu2+

Figure 5 Effect of adsorbents dosage on the percentage removal of Cd2+

## Effect of contact time

This parameter was studied at room temperature with a neutral pH, a concentration of 10ppm and the contact time ranging within 1min to 60 min. For nitrate and phosphate, 0.10g of absorbent was used and 0.20g for copper, lead and cadmium. This is an important parameter in the determination of the adsorption equilibrium time and adsorption kinetics.

According to several studies[24 & 25], the effect of contact time is observed with a rapid increase of percentage removal of the adsorbate in the first 10 to 20 minutes. Similarly, in this study it was observed from figure 4 to figure 7 that 99%, 96%, 96%, 75% and 100% respectively of nitrate, phosphate, lead, copper and cadmium were removed between 1 and 10 min. A very small change was observed from 10min to 20min and a very negligible change from 20 to 60min. Thus, the adsorption equilibrium was achieved at around 30min of contact time.

Figure 6 Effect of contact time on the percentage removal of NO3-

Figure 7 Effect of contact time on the percentage removal of PO43-

Figure 8 Effect of contact time on the percentage removal of Pb2+

Figure 9 Effect of contact time on the percentage removal of Cu2+

Figure 10 Effect of contact time on the percentage removal of Cd2+

## Effect of initial ion concentration

The effect of initial ion concentration was determined using 0.10g as initial dosage for nitrate and phosphate and 0.20g for lead, copper and cadmium. The working pH was 7, contact time was 30 minutes and the temperature was 298K. The concentration variation was between 10ppm to 100ppm.

The effect of initial ion concentration is observed by the decrease of percentage removal, as the initial concentration is increased. This happens normally after the adsorbent has reached saturation, meaning the sorption site on the adsorbents become less than the ions presents in the solution[26 & 27].  From figures 9, 10, 11 and 12 it was observed that up to 100 ppm, the different adsorbents kept their percentage removal at 100 % except for Copper, which percentage removal started decreasing just from 20 ppm. It was also observed in figures 13 that at 20 ppm, 50 ppm and 100ppm, the percentage removal respectively decreased at 99, 98 and 97 %.

Figure 11 Effect of NO3- initial concentration on its percentage removal

Figure 12 Effect of PO43- initial concentration on its percentage removal

Figure 13 Effect of Pb2+ initial concentration on its percentage removal

Figure 14 Effect of Cu2+ initial concentration on its percentage removal

Figure 15 Effect of Cd2+ initial concentration on its percentage removal

### Effect of temperature

This parameter was studied using the adsorbents dosage of 0.10g for nitrate and phosphate, and 0.20g for cadmium, lead and copper. The initial concentration was 10ppm, the pH was 7, the contact time was 30 minutes and the temperature varied between 298K and 353K.

This experiment, Figures 14, 15, 16, and 17, revealed that temperature had no effect on the adsorption study. In general, increasing the temperature reduces adsorption as the attractiveness between the adsorbent and the ions site of the adsorbate decreases[28]. However, this temperature is differ for different ions. Therefore, for lead in figure 15, it was observed that as the temperature increased from 298 k to 353k, the percentage removal decreased.

Figure 16 Effect of temperature on the percentage removal of NO3-

Figure 17 Effect of temperature on the percentage removal of PO43-

Figure 18 Effect of temperature on the percentage removal of Pb2+

Figure 19 Effect of temperature on the percentage removal of Cu2+

Figure 20 Effect of temperature on the percentage removal of Cd2+

### Effect of pH

This parameter was investigated at 298 K, 10 ppm concentration, and adsorbent dosages of 0.10 g for nitrate and phosphate and 0.20 g for lead, copper, and cadmium.

The pH is a crucial parameter in adsorption study. At different pH levels, different adsorbates and adsorbents respond differently. The alkali-treated clay mineral plays a major role as an adsorbent in the adsorption study. As in an acidic medium using an alkali-treated clay, both the medium and the adsorbate compete for the adsorbent active site. In a basic medium, there is a higher probability of a hydroxyl group formation [29]. In figure 20, where nitrate was used as an adsorbate in an acidic medium, the percentage removal was 27% this was significantly low compared to the percentage removal of the same adsorbate in an alkaline and neutral media, which was of 100%. The percentage removal of nitrate decreased in the acidic medium due to the saturation of the active site on the adsorbent. This was similar to phosphate figure 19, lead figure 20 and copper adsorbates figure 21. With Cadmium as an adsorbate figure 22, the pH did not affect the percentage removal.

Figure 21 Effect of pH on the percentage removal of NO3-

Figure 22 Effect of pH on the percentage removal of PO43-

Figure 23 Effect of pH on the percentage removal of Pb2+

Figure 24 Effect of pH on the percentage removal of Cu2+

Figure 25 Effect of pH on the percentage removal of Cd2+

CONCLUSION

After characterization, the unknown clay mineral from Mukurweini was identified as kaolinite 1A and the alkali thermal treated clay mineral as hydrosodalite sodium hexakis (alumino silicate). From the adsorption study, the percentage removal increased as the adsorbents dosage increased. 30 minutes of contact time was required to reach equilibrium. At 100 ppm concentration of the adsorbate, the percentage removal remained at 99.2%. The increase in temperature did not affect the adsorption study; however, the later was greatly affected by the change in pH.

References

- Haseena, M., Malik, M. F., Javed, A., Arshad, S., Asif, N., Zulfiqar, S., & Hanif, J. (2017). Water pollution and human health. Environmental Risk Assessment and Remediation, 1(3), 16-19. https://doi.org/10.4066/2529-8046.100020.

- Himansku Pathak, B.P. Bhatt, S.K Gupta. (2015). Water Pollution-Sources,Effects And Control. In H. Pathak, State of Indian Agricultural water. New Delhi: National Academy of Agricultural Sciences 7, 3528-3570.

- Hu, H., & Xu, K. (2020). Physicochemical technologies for HRPs and risk control. In H. Ren & X. Zhang (Eds.), High-Risk Pollutants in Wastewater (pp. 169-207). Elsevier. https://doi.org/10.1016/B978-0-12-816448-8.00008-3

- Hartwig, A. (2013). Cadmium and cancer. In Metal ions in life sciences (Vol. 11, pp. 491-507). https://doi.org/10.1007/978-94-007-5179-8_15

- Mateo-Sagasta, J., Marjani Zadeh, S., & Turral, H. (2017). Water pollution from agriculture: A global review. Food and Agriculture Organization of the United Nations. https://www.fao.org/3/i7754e/i7754e.pdf

- Selim, M. M. (2020). Introduction to the Integrated Nutrient Management Strategies and Their Contribution to Yield and Soil Properties. International Journal of Agronomy. https://doi.org/10.1155/2020/2821678

- Shah Jahan Leghari, Niaz Ahmed,Mustafa Laghari, Abdul HafeezLaghar,Ghulam Mustafa Bhabhan,. (2016). Role of Nitrogen for Plant Growth and Development. advance in Environmental Biology 9(10): 209-218.

- Bryan, N. S., & van Grinsven, H. (2013). The role of nitrate in human health. Advances in Agronomy, 119, 153-182. https://doi.org/10.1016/B978-0-12-407247-3.00003-2

- Majumdar, D. (2003). The blue baby syndrome: Nitrate poisoning in humans. Resonance, 8(10), 20-30. https://doi.org/10.1007/BF02840703

- Ansari, A. A., Gill, S. S., Lanza, G. R., & Rast, W. (Eds.). (2011). Eutrophication: Causes, Consequences and Control. Springer. https://doi.org/10.1007/978-90-481-9625-8

- Khan, T. A. (2011). Trace Elements in the Drinking Water and Their Possible Health Effects in Aligarh City, India. Journal of Water Resource and Protection. https://doi.org/10.4236/jwarp.2011.37062

- World Health Organization. (2011). Arsenic in Drinking-water: Background document for development of WHO Guidelines for Drinking-water Quality. https://www.who.int/publications/i/item/9789241548116

- Yamasaki, H., Pilon, M., & Shikanai, T. (2008). How do plants respond to copper deficiency? Plant Signal Behavior, 3(4), 231-232. https://doi.org/10.4161/psb.3.4.5094

- National Research Council (US) Committee on Copper in Drinking Water. (2000). Copper in Drinking Water. National Academies Press (US). https://doi.org/10.17226/9782

- Debnath, B., Singh, W. S., & Manna, K. (2019). Sources and toxicological effects of lead on human health. Indian Journal of Medical Specialities, 10(2), 66-71. https://doi.org/10.4103/INJMS.INJMS_30_18

- Assi, M. A., Hezmee, M. N. M., Haron, A. W., Sabri, M. Y., & Rajion, M. A. (2016). The detrimental effects of lead on human and animal health. Veterinary World, 9(6), 660-671. https://doi.org/10.14202/vetworld.2016.660-671

- Cannata, M. G., Carvalho, R., Bertoli, A. C., Augusto, A. S., Bastos, A. R. R., Carvalho, J. G., & Freitas, M. P. (2013). Effects of Cadmium and Lead on Plant Growth and Content of Heavy Metals in Arugula Cultivated in Nutritive Solution. Communications in Soil Science and Plant Analysis, 44(5), 952-961. https://doi.org/10.1080/00103624.2013.753700

- Králik, M. (2014). Adsorption, chemisorption, and catalysis. Chemical Papers, 68(12), 1625–1638. https://doi.org/10.2478/s11696-014-0624-9

- Fowler, B. A., Alexander, J., & Oskarsson, A. (2015). Toxic Metals in Food. In G. F. Nordberg, B. A. Fowler, & M. Nordberg (Eds.), Handbook on the Toxicology of Metals (4th ed., pp. 123-140). Academic Press. https://doi.org/10.1016/B978-0-444-59453-2.00006-8

- Rafati Rahimzadeh, M., Rafati Rahimzadeh, M., Kazemi, S., & Moghadamnia, A.-A. (2017). Cadmium toxicity and treatment: An update. Caspian Journal of Internal Medicine, 8(3), 135-145. https://doi.org/10.22088/cjim.8.3.135

- Suresh Guptaa and B V Babu. (2006). Adsorption of Cr(VI) by a Low-Cost Adsorbent Prepared from Neem Leaves. National Conference on Environmental Conservation, 175-180.

- Wang, F. Y., Wang, H., & Ma, J. W. (2010). Adsorption of cadmium (II) ions from aqueous solution by a new low-cost adsorbent--bamboo charcoal. Journal of Hazardous Materials, 177(1-3), 300-306. https://doi.org/10.1016/j.jhazmat.2009.12.032

- Padmavathy, K. S., Madhu, G., & Haseenaa, P. V. (2016). A study on Effects of pH, Adsorbent Dosage, Time, Initial Concentration and Adsorption Isotherm Study for the Removal of Hexavalent Chromium (Cr (VI)) from Wastewater by Magnetite Nanoparticles. Procedia Technology, 24, 585-594. https://doi.org/10.1016/j.protcy.2016.05.127

- Hu, H., & Xu, K. (2020). Chapter 8 - Physicochemical technologies for HRPs and risk control. In X. Zhang & H. Ren (Eds.), High-Risk Pollutants in Wastewater (pp. 169-207). Elsevier. https://doi.org/10.1016/B978-0-12-816448-8.00008-3

- Hartwig, A. (2013). Cadmium and cancer. Metal ions in life sciences 11, 491-507. https://doi.org/10.1007/978-94-007-5179-8_15

- Ye, R., Zhao, M., Mao, X., Wang, Z., Garzón, D. A., Pu, H., Zhao, Z., & Chen, P. (2021). Nanoscale cooperative adsorption for materials control. Nat Commun, 12(1), 4287. https://doi.org/10.1038/s41467-021-24590-y

- Olarinde, M. G., Agenuma, A. M., Joseph, A. O., & Abosede, A. (2019). Environmental health status of some aquatic ecosystems in Badagry Division, Lagos, Nigeria. International Journal of Ecotoxicology and Ecobiology, 4(4), 93-102. https://doi.org/10.11648/j.ijee.20190404.13

- Youcef, L. D., Belaroui, L. S., & López-Galindo, A. (2019). Adsorption of a cationic methylene blue dye on an Algerian palygorskite. Applied Clay Science. https://doi.org/10.1016/j.clay.2019.105145

- Gamoudi, S., & Srasraa, E. (2019). Adsorption of organic dyes by HDPy+-modified clay: Effect of molecular structure on the adsorption. Journal of Molecular Structure, 1193, 522-531. https://doi.org/10.1016/j.molstruc.2019.05.055

- Gorzin, F., & Bahri Rasht Abadi, M. M. (2018). Adsorption of Cr(VI) from aqueous solution by adsorbent prepared from paper mill sludge: Kinetics and thermodynamics studies. Adsorption Science & Technology, 36(1-2), 149-169. https://doi.org/10.1177/0263617416686976

- Al Mayyahi, A., & Al-Asadi, H. A. A. (2018). Advanced Oxidation Processes (AOPs) for Wastewater Treatment and Reuse: A Brief Review. Asian Journal of Applied Science and Technology, 2(3), 18-30. http://www.ajast.net/volume-2-issue-3/

- Wei, M., Zeng, Y., Zou, L., & Xu, S. (2019). Analysis of the Influence of Water-Vapor Correction Term on the Measurement Uncertainty of Wind Speed. MAPAN, 34, 333-343. https://doi.org/10.1007/s12647-019-00338-4

- Eshraq, B. K., Mona, A. M., Sayed, A. F., & Emam, A. A. (2016). Effect of Soaking, Cooking and Germination on Chemical Constituents and Bioactive Compounds as well as their Cytotoxic Activities of Black Bean Extracts. Nat Prod Chem Res, 4(6), 237. https://doi.org/10.4172/2329-6836.1000237