Original Research Article

Characterization of Soft Soil Strength Properties and Settlement Behavior

.

ABSTRACT

Background: Soft soils pose significant challenges in construction projects because of their high compressibility and low shear strength, leading to excessive settlement and structural instability. Aims: This study, uniquely integrates experimental characterization with advanced statistical modeling to provide a comprehensive understanding of soft soil behavior. Specifically, it introduces a novel framework that combines principal component analysis (PCA) with regression modeling to identify dominant settlement-influencing factors and predict settlement under various loading conditions. Methodology: Soil samples were collected from predetermined sites and tested in the laboratory to determine key geotechnical parameters, including moisture content (MC), optimum moisture content (OMC), cohesion (C), internal friction angle (∅), unconfined compressive strength (UCS), void ratio (e), and compressibility characteristics. Consolidation tests assessed settlement tendencies, while PCA identified the parameters with the greatest influence on soil performance. Regression modeling was then applied to develop a predictive tool for estimating settlement based on these characteristics. Results: The results revealed that moisture content, void ratio, and compression index were the most critical factors controlling settlement. Regression analysis confirmed strong correlations between these parameters and measured settlement, while PCA highlighted the dominance of cohesiveness and compactness in influencing soil response. The integration of PCA and regression thus provided both explanatory and predictive insights, demonstrating a methodological advancement in soft soil characterization. Conclusion: This study contributes to geotechnical knowledge by not only characterizing problematic soft soils but also presenting an innovative analytical approach for predicting settlement. The combined regression–PCA framework offers engineers a practical decision-support tool for foundation design and risk mitigation in soft soil environments..

Keywords: Soft Soil, Settlement, Regression Analysis

1. INTRODUCTION

Soft soils such as normally consolidated clays, silts, peats, and organic deposits are widely acknowledged for their problematic behavior in geotechnical engineering due to their high-water content, low undrained shear strength, and significant compressibility (Liu et al., 2019; Ural, 2018; Varghese et al., 2021). Their structure is often sensitive to stress changes and loading history, making them susceptible to large and prolonged settlements (Harshit, and Abhivek, 2024; Nguyen, 2024; Onyelowe et al., 2023). These intrinsic weaknesses pose serious challenges in construction, particularly in coastal and deltaic regions where soft deposits are common (Amadi, 2022; Mbevo Fendoung, and Hubert-Ferrari, 2025).

Construction on soft soils often encounters significant difficulties due to their inherent low strength and high compressibility (Gue and Gue, 2022; Lin et al., 2022; Lin et al., 2019; Mohamad et al., 2016). These properties lead to considerable settlement and stability issues, which can compromise the safety and longevity of structure (Feng et al., 2022. In many regions around the world, especially in coastal areas and river deltas, soft soils are prevalent, necessitating accurate and reliable methods for predicting their behavior under load (Gue and Gue, 2022; Mohamad et al., 2016; Xiao et al., 2022).

Researchers have shown that fabric and microstructural arrangements, such as flocculated clay platelets or fibrous peat matrices, strongly influence compressibility and shear strength (Diaz-Rodriguez and Gonzalez-Rodriguez, 2013; O’Kelly and Pichan, 2013). Consequently, disturbance during sampling and testing can drastically reduce measured strength parameters, leading to conservative or misleading design inputs.

Predicting the behavior of structures built on these soils remains a challenge due to the complex interactions between soil properties and loading conditions (Wang et al., 2022; Wang et al., 2023). Traditional methods of soil assessment may not provide sufficient accuracy, leading to design and construction issues such as excessive settlement, foundation instability, and even structural failure. Traditional methods of soil assessment often fall short in providing the accuracy required for effective design and construction, particularly in geotechnical engineering (Dematte et al., 2019). Traditional geotechnical methods for characterizing soft soil properties, including laboratory tests and empirical correlations, often face limitations due to the complex, variable nature of these soils (Chen et al., 2023).

Settlement prediction in soft soils remains a complex issue due to the combined effects of primary consolidation, secondary compression, and creep. Terzaghi’s classical consolidation theory provides the foundational framework for estimating primary settlement; however, its assumptions of linear compressibility and one-dimensional drainage are often restrictive. The settlement behavior of soft soils is better captured through the e–logσ′ relationship, with compression index (Cc) and recompression index (Cr) being central parameters. In highly organic soils, secondary compression is especially pronounced, with long-term settlement persisting after pore water dissipation. Mesri’s concept of a relatively constant Cα/Cc ratio has been widely applied in practice to estimate creep settlements. For peats and organic clays, whose fibrous microstructure governs drainage and deformation, empirical extrapolation from conventional clay models is inadequate, prompting researchers to propose specialized compressibility frameworks.

The inherent heterogeneity, coupled with spatial and temporal variations, complicates the prediction of settlement and shear strength, making it difficult to ensure the stability and durability of structures built on soft soils (Zhao et al., 2024). This inadequacy can lead to significant issues such as excessive settlement, foundation instability, and even structural failure (Feng et al., 2020). Furthermore, these methods can be time-consuming and resource-intensive, often leading to conservative designs that increase construction costs and material usage.

There is a critical need for a more robust and precise approach to characterize the strength properties and predict the settlement behavior of soft soils. Such an approach would not only enhance the safety and reliability of geotechnical designs but also optimize construction processes, reduce costs, and minimize risks associated with structural failures. This necessitates a thorough investigation into the strength and settlement characteristics of soft soils to develop better predictive tools and construction techniques. Recent years have also witnessed growing interest in data-driven and regression-based methods for settlement prediction. Traditional linear regression has been extended to multivariate and non-linear models, capturing complex relationships between soil properties, construction conditions, and settlement outcomes. This research aims to address this need by employing regression analysis to develop predictive models based on empirical data from comprehensive soil testing.

The specific objectives this study addresses is characterizing key geotechnical properties of soft soils relevant to settlement; identifying the dominant parameters influencing settlement using PCA; and developing an empirical regression model to predict settlement based on these parameters. The research gap addressed here lies in the lack of predictive tools that integrate routine soil characterization with statistical modeling to quantify settlement behavior in local soft soils. Existing studies often focus on either (a) laboratory characterization without predictive modeling, or (b) empirical settlement models without statistical validation. Our study bridges this gap by systematically linking soil index/engineering properties with settlement behavior through a combined PCA–regression framework.

2. methodology

The methodology for this study involved a series of practical steps aimed at collecting, analyzing, and modeling data to characterize the strength properties and settlement behavior of soft soils. The process was divided into five main phases: data collection, laboratory testing, data analysis, model development, and validation. Multiple sites with prevalent soft soils, such as clays, silts, and organic soils, were identified, to ensure a range of soil types and conditions to cover various geographical regions and soil characteristics. The soil samples were obtained from 3 sites from different locations within Ibadan North. Two (2) trial pits were considered, and samples were obtained at depths of 0.5m and 1m, a from each trial pits. The soil samples were obtained as undisturbed soil samples, carefully packed in sealed containers to prevent contamination and moisture losses, and then transported to the laboratory.

Laboratory analysis was carried out to determine the properties of the soil samples. These analyses included the determination of natural moisture content, and void ratio; and determination of shear strength, UCS, permeability, and Compaction tests to produce a model for predicting the soil settlement and consolidation. Physical properties tests were conducted to determine the essential characteristics of the soil that influence its behavior under various conditions. These tests provide fundamental data required for the classification, analysis, and engineering design of soil structures.

All tests were carefully chosen following recognized international standards (ASTM/BS/IS), and each test was selected to capture specific soil characteristics relevant to settlement behavior. Where applicable the following standards were used: ASTM D2216 / BS 1377 (Part 2) for moisture content, ASTM D4318 / BS 1377 for Atterberg limits, ASTM D3080 / BS 1377 (Part 7) for direct shear, ASTM D2166 for unconfined compressive strength (UCS), ASTM D2435 / BS 1377 (Part 5) for consolidation, ASTM D5084 / ASTM D2434 for permeability and ASTM D1883 for CBR (where applied). Where a standard provides multiple acceptable procedures, the specific clause used is stated in each test subsection below. Sampling, specimen preparation, instrumentation and test execution followed the cited standards to maximise reproducibility.

2.1 Sampling Plan and Geological Content

Soil samples were obtained from 6 boreholes drilled from 3 locations within the study area at Ibadan North. The study area lies within a depositional environment characterized by recent alluvial and residual soils, typical of low-lying terrain influenced by seasonal flooding and groundwater fluctuations. The geological profile is dominated by soft clays and silty layers interbedded with occasional sandy seams, reflecting fluvio-lacustrine depositional processes. This geological context explains the high plasticity, compressibility, and variable strength properties observed in the tested soils. The shallow groundwater table further contributes to the soils’ low effective stress and high settlement potential. The boreholes were advanced to depths of 0.5m and 1m and representative disturbed and undisturbed samples were collected from each identified stratum. These depths were chosen because the study primarily targeted shallow foundation conditions where soft soil poses immediate settlement risks. This depth was selected to represent the soil strata relevant to shallow foundation applications, where soft soils often exert the most immediate influence on settlement behavior.

2.2 Sampe Handling and Laboratory Replication

All undisturbed samples were sealed immediately in plastic film and labelled. Replication: where material volume permitted, at least three replicates were prepared for index tests (moisture content, Atterberg limits) and two to three undisturbed specimens were tested for engineering property tests (consolidation, UCS).

2.2.1 Moisture Content Analysis

Moisture content is the amount of water present in the soil, expressed as a percentage of the weight of the dry soil. This property is crucial for understanding the soil's behavior and consistency. The test was conducted in accordance with ASTM D2216 / BS 1377 (Part 2, 1990). To determine moisture content, a representative portion of the soil sample was weighed, dried in an oven, and weighed again. The test was conducted to determine the moisture content in a soil material relative to its dry weight. Moisture content determination is a critical measurement used to quantify the amount of water present in soil. It is expressed as the ratio of the mass of water in a soil sample to the dry soil mass of a given soil sample, usually represented as a percentage. This measurement is essential for understanding the physical properties and behaviors of soil materials in fields of construction.

Equipment used includes Oven, Sensitive weighing balance, Air-tight containers.

Procedures:

a.	Soil sample was placed in the air-tight container.

b.	The container with the soil sample was weighted (W1).

c.	The container with soil was placed in an oven and dried at 105℃ - 110℃ for 24 hours.

d.	The container was removed from the oven and was allowed to cool in a desiccator.

e.	The container with the dried soil sample was weighted (W2).

f.	Moisture content was calculated using Eqn. 1

Moisture Content = W1- W2W2   x 100%					…Eqn. 1

Where:

W1 	=	Weight of container with soil sample,

W2	=	Weight of container with the dried sample

2.2.2 Void Ratio

The void ratio is a measure of the volume of voids (air and water spaces) to the volume of solids in the soil. This test involves determining the bulk density and the particle density of the soil. Bulk density and specific gravity were determined in accordance with ASTM D854 / BS 1377 (Part 2). Dry bulk density (dry mass per total volume) was measured using standard sample trimming and volume measurement procedures. The void ratio is crucial for understanding the porosity and compressibility of the soil.

Equipment used includes Oven, Balance sensitive to 0.01 gm, Graduated cylinder or pycnometer, Distilled water.

Procedure:

a.	The bulk density (ρ) of the soil sample was obtained.

b.	Particle density (Gs) was determined using a pycnometer or graduated cylinder filled with distilled water and soil particles.

c.	Void ratio (e) was calculated using Eqn.2.

Void ratio, e = GsPwPd-1							…Eqn. 2

Where:

e	=	Void ratio

Gs	=	Specific gravity of soil

ρd	=	Dry dulk density of soil sample

ρw	=	Density of water (typically 1000kg-3 at 4℃)

2.2.3 Shear Strength Test

The direct shear test measures the shear strength of soil by placing a soil sample in a shear box and applying a horizontal force until the sample fails. It was conducted in accordance with ASTM D3080 / BS 1377 (Part 7) to determine shear stress under different normal stresses. The test provides data on the shear stress and the corresponding normal stress. It is straightforward and provides valuable information about soil's frictional properties. The direct shear strength test was conducted to provide comparative strength parameters under drained conditions for granular and mixed samples. The direct shear provides frictional parameters (c′, φ′) under specified drainage conditions.

The direct shear test was employed in accordance with ASTM D3080 / BS 1377 (Part 7), as it provides comparative shear strength parameters under controlled laboratory conditions.

Equipment required includes: Direct shear box apparatus, loading frame, proving ring, dial gauges for vertical and horizontal displacement, Water bath (if required).

Procedure:

a.	Soil specimen of known dimensions was prepared and placed in the shear box.

b.	A normal load was applied to the soil specimen.

c.	The dial gauges was set to zero

d.	A horizontal load was applied to the soil specimen at a constant rate of strain until failure occurs.

e.	The shear force and corresponding horizontal displacement was recorded

f.	The test for different normal loads was repeated.

2.2.4 Unconfined Compressive Strength of Soil Samples

To address the limitations of the direct shear test, we complemented it with the Unconfined Compressive Strength (UCS) test (ASTM D2166 / IS 2720 Part 10), which is more suitable for cohesive soils and provided reliable estimates of undrained shear strength. The unconfined compression test is a simple method to determine the undrained shear strength of cohesive soils. The test was performed following ASTM D2166 / IS 2720 (Part 10). A cylindrical soil sample is compressed axially until failure without any lateral confinement. The maximum axial stress at failure is the unconfined compressive strength. This test is quick and useful for cohesive soils like clays.

Equipment required includes: Compression testing machine and Dial gauges or electronic displacement transducers.

Procedure:

a.	A cylindrical soil specimen was prepared.

b.	The specimen was placed in the compression testing machine.

c.	Compressive load at a constant rate of strain was applied until failure occurs.

d.	The compressive load and corresponding axial displacement was recorded.

2.2.5 Permeability of Soil Samples

The permeability test measures the rate at which water flows through soil. It can be conducted using a constant head or falling head permeameter. The coefficient of permeability was determined using falling head and constant head permeameters, depending on sample characteristics, in accordance with ASTM D2434 (constant head) / ASTM D5084 (falling head). The test involves saturating the soil sample, applying a hydraulic gradient, and measuring the volume of water that flows through the soil over a specified period. The permeability coefficient is calculated to understand the soil's ability to transmit water, which is crucial for drainage and groundwater studies.

Equipment Required includes: Permeameter (constant head or falling head), Stop watch, Graduated cylinder, Balance sensitive to 0.01 gm.

Procedure:

a.	The soil sample was saturated in the permeameter.

b.	A constant head of water was maintained.

c.	The quantity of water collected (Q) in the graduated cylinder over a specific time interval (t) was measured.

d.	The cross-sectional area (A) and length (L) of the soil sample were measured.

e.	Coefficient of permeability (k) was calculated using the formula in Eqn. 3

k = (Q * L) / (A * h * t), where h is the constant head.		… Eqn.3

2.2.6 Consolidation of Soil Samples

The compressibility test determines how much a soil sample compresses under load, reflecting its settlement behavior. One-dimensional consolidation tests were carried out using an oedometer in accordance with ASTM D2435 / BS 1377 (Part 5).. A soil specimen is placed in an oedometer and subjected to incremental loading. The vertical displacement is measured for each load increment. Consolidation tests were carried out on undisturbed samples in an oedometer cell following ASTM D2435. Specimen size and preparation followed the standard. A logarithmic loading schedule (equal ratio increments) was adopted to define the compression curve; a typical example schedule used in this study was: 12.5, 25, 50, 100, 200, 400 kPa (final maximum stress chosen to bracket the expected field vertical effective stress). Each increment was maintained until primary consolidation was judged complete. Primary consolidation completion criterion: either (a) the specimen reached approximately 90% consolidation (t90_{90}90​) as determined from the logarithmic time method, or (b) vertical deformation between successive time intervals became smaller than 0.01 mm/hour for a sustained period — whichever criterion was most appropriate for the sample. From the consolidation curve the compression index Cc​, recompression index Cr​, and preconsolidation pressure pc​ were determined.The results are used to plot a graph of void ratio versus effective stress, from which the compression index and recompression index are derived. This test is essential for predicting soil settlement under foundation loads.

Equipment required includes: Oedometer apparatus, loading frame, Dial gauges for vertical displacement, Water bath (if required).

Procedure:

a.	Soil specimen was prepared and placed in oedometer ring.

b.	Initial load was applied and the specimen was allowed to consolidate under this load until primary consolidation is completed

c.	Vertical displacement was measured at regular intervals.

d.	Additional loads were applied in increments and the consolidation process for each load increment was repeated.

e.	The vertical displacement for each load increment was recorded.

2.2.7 California Bearing Ratio Test

The California Bearing Ratio (CBR) test determines the load-bearing capacity of a soil specimen, expressed as a ratio of the applied load to a standard load at specific penetration depths. The CBR test was performed to evaluate the load-bearing capacity of compacted soil specimens, in accordance with ASTM D1883 / IS 2720 (Part 16). The test evaluated soil strength for designing pavement subgrades and base materials. The CBR test is primarily designed to assess pavement subgrade strength under penetration loading and though it is not a recognised predictor of vertical settlement beneath foundations. The CBR test was conducted for contextual completeness but excluded it from statistical modelling.

Equipment required includes: CBR testing machine with a loading frame, Penetration plunger (with a standard diameter of 50 mm), Molds (152 mm diameter and 175 mm height) with collar and base plate, Spacer disk, Compaction rammer, measuring dial gauges (for load and penetration)., Weighing balance, Soaking tank (if required), Sieve (4.75 mm) and mixing tools for sample preparation.

Procedure:

a.	Obtained was the soil passing through a 20 mm sieve.

b.	The soil with the required water content (optimum moisture content for compacted samples) was mixed.

c.	Spacer disk was placed at the bottom of the mold.

d.	The soil in the mold was compacted in 3 or 5 layers using a standard or modified proctor compaction method, ensuring uniform density.

e.	The surface was levelled and the collar and base plate were attached.

f.	For soaked samples, the mold was placed in a soaking tank for 4 days and was maintained under water with a surcharge weight.

g.	The mold was removed from the soaking tank, and excess water was drained.

h.	The mold was placed in the testing machine, and proper alignment was ensured.

i.	The plunger was centrally on the specimen.

j.	Vertical load was applied at a penetration rate of 1.25 mm/min.

k.	The loads corresponding to penetrations of 0.25, 0.50, 0.75, 1.00, 1.25, 1.50, 2.00, and 2.50 mm were recorded.

l.	The load per unit area (stress) for specific penetration depths was determined.

m.	The stresses with standard values (13.24 kN at 2.50 mm and 19.96 kN at 5.00 mm) were compared.

n.	The CBR was calculated using the formula in Eqn 4

CBR = Measured StressStandard stress x 100		… Eqn.4

2.3 Data Analysis

Principal Component Analysis (PCA) and multiple regression were used to identify dominant parameters and build empirical relationships for settlement prediction. Given the limited number of undisturbed specimens available from each stratum, the following precautions were taken to improve robustness: All predictor variables were standardised before PCA. The number of PCA components retained was chosen based on the scree plot and cumulative variance explained (>80%).

For regression model validation we used cross-validation (leave-one-out or k-fold, depending on sample size) and report adjusted R2R^2R2, root-mean-square error (RMSE) and p-values for predictors. All model assumptions (linearity, normality of residuals, variance homogeneity) were tested and reported. Where assumptions were violated, non-parametric alternatives or variable transformations were used.

2.3.1 Regression Analysis

Regression analysis is a statistical method used to model the relationship between a dependent variable and one or more independent variables. It helps in predicting the dependent variable based on the values of the independent variables. In soil testing, regression analysis can develop predictive models for soil behavior based on physical properties.

3. results and discussion

3.1 Soil Characterization

3.1.1 Moisture Content

The moisture content of the soil samples in table 1, shows noticeable variation across the different locations, depths, and trial pits, indicating spatial variability and heterogeneity in the soil profile.

Table 1: Natural Moisture Content of Soil Samples

| Location | Trial Pit | Depth | Moisture content |
| --- | --- | --- | --- |
| Loc 1 | TP 1 | 0.5m | 17.7 |
| Loc 1 | TP 1 | 1.0m | 14.7 |
| Loc 1 | TP 2 | 0.5m | 17.7 |
| Loc 1 | TP 2 | 1.0m | 14.6 |
| Loc 2 | TP 1 | 0.5m | 17.8 |
| Loc 2 | TP 1 | 1.0m | 20.0 |
| Loc 2 | TP 2 | 0.5m | 22.2 |
| Loc 2 | TP 2 | 1.0m | 22.1 |
| Loc 3 | TP 1 | 0.5m | 18.0 |
| Loc 3 | TP 1 | 1.0m | 11.4 |
| Loc 3 | TP 2 | 0.5m | 18.6 |
| Loc 3 | TP 2 | 1.0m | 27.5 |

At Location 1, the moisture content decreases consistently with depth, from 17.7% at 0.5 m to approximately 14.6–14.7% at 1 m in both trial pits. This behavior aligns with the typical trend in many soils where deeper layers have reduced moisture due to compaction, consolidation, and reduced surface water infiltration. The reduced moisture in deeper layers often suggests more stable soil properties in terms of settlement and shear strength, critical for geotechnical considerations.

In Location 2, a contrasting trend is observed, where the moisture content increases with depth. At 0.5 m, moisture content ranges between 17.8% and 22.2%, while at 1 m, it is around 20.0% (estimated) to 22.1%. This pattern may indicate the presence of groundwater or fine-grained materials with higher water retention capacity in the deeper layers. The higher moisture levels in this location can adversely affect soil strength, leading to increased compressibility and potential settlement under loading.

Location 3 exhibits significant variability, particularly at 1 m depth, where Trial Pit 1 shows a low moisture content of 11.4% compared to 27.5% in Trial Pit 2. At 0.5 m, moisture for Trial Pit 1 (18.0%) is slightly lower than the measured value for Trial Pit 2 (18.6%). This variability suggests the presence of different soil types or conditions between the trial pits. Trial Pit 1 might have encountered coarser or drier materials, while Trial Pit 2 could have encountered more saturated or finer-grained soil. Such variability highlights the complexity of soft soils and emphasizes the need for site-specific investigations.

The variation across locations and depths suggests that localized soil conditions and environmental factors, such as water table depth and soil composition, significantly influence moisture levels.

3.1.2 Void Ratio of Soil Samples

The void ratio results shown in table 2, demonstrate a marked variation across different locations and depths, reflecting the soil's inherent composition and compressibility.

Table 2.	Initial and Void Ratio of soil Samples at different locations

| Location | Trial Pit | Depth | Initial void ratio eo | Final void ratio, e |
| --- | --- | --- | --- | --- |
| Loc 1 | TP 1 | 0.5m | 0.352 | 0.293 |
| Loc 1 | TP 1 | 1.0m | 0.328 | 0.195 |
| Loc 1 | TP 2 | 0.5m | 0.326 | 0.240 |
| Loc 1 | TP 2 | 1.0m | 0.345 | 0.268 |
| Loc 2 | TP 1 | 0.5m | 0.335 | 0.238 |
| Loc 2 | TP 1 | 1.0m | 0.336 | 0.215 |
| Loc 2 | TP 2 | 0.5m | 0.332 | 0.198 |
| Loc 2 | TP 2 | 1.0m | 0.338 | 0.187 |
| Loc 3 | TP 1 | 0.5m | 0.373 | 0.018 |
| Loc 3 | TP 1 | 1.0m | 0.373 | 0.334 |
| Loc 3 | TP 2 | 0.5m | 0.345 | 0.287 |
| Loc 3 | TP 2 | 1.0m | 0.318 | 0.249 |

At Location 1, the void ratio values are relatively low, indicating denser soil with minimal air or water-filled void spaces, suggesting a higher load-bearing capacity and reduced potential for significant volume changes under applied loads. In contrast, Location 2 exhibits high initial void ratios, characteristic of soft clayey soils, where large void spaces result in higher compressibility and a greater likelihood of settlement under loading. Location 3 presents variable trends in void ratio, indicating a heterogeneous soil composition with alternating layers of coarse and fine-grained materials. The reduction in void ratio after consolidation highlights the susceptibility of high-void soils, such as those in Location 2, to substantial settlement, whereas denser soils in Location 1 exhibit comparatively minor reductions.

3.1.3 Compaction Tests

The compaction results in table 3 revealed the maximum dry density (MDD) and optimum moisture content (OMC) of the soils, which directly influence their load-bearing capacity.

Table 3. Optimum moisture content and maximum dry density of soil samples at different location

| Location | Trial Pit | Depth | OMC (%) | MDD (kg/m3) |
| --- | --- | --- | --- | --- |
| Loc 1 | TP 1 | 0.5m | 16.6 % | 1737.0 kg/m3 |
| Loc 1 | TP 1 | 1.0m | 15.5 % | 1760.0 kg/m3 |
| Loc 1 | TP 2 | 0.5m | 10.0 % | 1837.0 kg/m3 |
| Loc 1 | TP 2 | 1.0m | 9.6 % | 1828.0 kg/m3 |
| Loc 2 | TP 1 | 0.5m | 13.5 % | 1687.0 kg/m3 |
| Loc 2 | TP 1 | 1.0m | 11.3 % | 1797.0 kg/m3 |
| Loc 2 | TP 2 | 0.5m | 17.0 % | 1603.0 kg/m3 |
| Loc 2 | TP 2 | 1.0m | 16.3 % | 1605.0 kg/m3 |
| Loc 3 | TP 1 | 0.5m | 11.5 % | 1838.0 kg/m3 |
| Loc 3 | TP 1 | 1.0m | 10.5 % | 1860.0 kg/m3 |
| Loc 3 | TP 2 | 0.5m | 16.2 % | 1688.0 kg/m3 |
| Loc 3 | TP 2 | 1.0m | 19.5 % | 1616.0 kg/m3 |

At Location 1, the high MDD and relatively low OMC indicate denser soils that can support significant structural loads with minimal settlement. In Location 2, the low MDD and high OMC reflect clay-dominated soils with high water demand for effective compaction. These soils require precise control of water content during compaction to enhance their strength and stability. Location 3 exhibits variability in both MDD and OMC, signifying inconsistent soil composition. Achieving optimum compaction in heterogeneous soils can be challenging but is essential to minimize settlement and improve foundation stability.

3.1.4 Shear Strength of Soil Samples

Shown in table 4, the shear strength results illustrate the soil’s resistance to deformation and shear stress under loading.

Table 4. Cohesion, angle of shearing resistance and direct shear strength of soil samples at different locations

| Location | Trial Pit | Depth | Apparent Cohesion C’ | Angle of shearing Resistance | Direct Shear strength |
| --- | --- | --- | --- | --- | --- |
| Loc 1 | TP 1 | 0.5m | 5 kPa | 36° | 150.3085kPa |
| Loc 1 | TP 1 | 1.0m | 90.0 kPa | 8.5° | 119.8902kPa |
| Loc 1 | TP 2 | 0.5m | 53.9 kPa | 12.0° | 96.41131kPa |
| Loc 1 | TP 2 | 1.0m | 38.2kPa | 28.6° | 147.2435kPa |
| Loc 2 | TP 1 | 0.5m | 33.6 kPa | 25.0° | 126.8615kPa |
| Loc 2 | TP 1 | 1.0m | 13.5 kPa | 34.0° | 148.4017kPa |
| Loc 2 | TP 2 | 0.5m | 58.6 kPa | 26.8° | 159.6273kPa |
| Loc 2 | TP 2 | 1.0m | 56.8 kPa | 14.5° | 108.5235kPa |
| Loc 3 | TP 1 | 0.5m | 21.0 kPa | 38.0° | 177.2571kPa |
| Loc 3 | TP 1 | 1.0m | 19.0 kPa | 38.0° | 175.2571kPa |
| Loc 3 | TP 2 | 0.5m | 41.0 kPa | 17.0° | 102.1461kPa |
| Loc 3 | TP 2 | 1.0m | 43.1 kPa | 27.0° | 145.0051kPa |

Location 1 shows relatively high shear strength values, consistent with its low moisture content and dense composition, making it ideal for construction. Location 2, however, demonstrates significantly lower shear strength, especially at greater depths, due to its high moisture content and clay-dominated composition. This reduction in shear strength poses challenges for structural stability and requires interventions such as soil stabilization. Location 3 exhibits variable shear strength across depths, reflecting its mixed soil types, where finer-grained materials reduce strength while coarser materials increase it.

3.1.5 Unconfined Compressive Strength (UCS) of Soil Samples

Shown in table 5, the UCS results gotten show the soil's ability to withstand axial loads without lateral confinement.

Table 5.	Unconfined compressive strength of soil samples

| Location | Trial Pit | Depth | UCS |
| --- | --- | --- | --- |
| Loc 1 | TP 1 | 0.5m | 45.2 kPa |
| Loc 1 | TP 1 | 1.0m | 35.0 kPa |
| Loc 1 | TP 2 | 0.5m | 34.5 kPa |
| Loc 1 | TP 2 | 1.0m | 39.5 kPa |
| Loc 2 | TP 1 | 0.5m | 25.0 kPa |
| Loc 2 | TP 1 | 1.0m | 25.0 kPa |
| Loc 2 | TP 2 | 0.5m | 49.7 kPa |
| Loc 2 | TP 2 | 1.0m | 29.8 kPa |
| Loc 3 | TP 1 | 0.5m | 39.5 kPa |
| Loc 3 | TP 1 | 1.0m | 44.2 kPa |
| Loc 3 | TP 2 | 0.5m | 49.1 kPa |
| Loc 3 | TP 2 | 1.0m | 63.1 kPa |

Location 1 achieves higher UCS values, indicative of denser soils with better structural integrity. On the other hand, Location 2 exhibits very low UCS, reflective of its soft, clay-rich composition, which is highly compressible and prone to significant settlement under load. Location 3 shows varied UCS values, consistent with the presence of heterogeneous layers. The results emphasize the unsuitability of soft soils in Location 2 for bearing substantial loads unless stabilized, while soils in Location 1 are more reliable for construction.

3.1.6 Permeability of Soil Samples

The permeability results in table 6 shows the rate at which water can flow through the soil matrix.

Table 6.	Permeability of soils samples at different location

| Location | Trial Pit | Depth | Permeability, K (cm/s) |
| --- | --- | --- | --- |
| Loc 1 | TP 1 | 0.5m | 0.00001005 |
| Loc 1 | TP 1 | 1.0m | 0.00000896 |
| Loc 1 | TP 2 | 0.5m | 0.00001483 |
| Loc 1 | TP 2 | 1.0m | 0.00001287 |
| Loc 2 | TP 1 | 0.5m | 0.00001207 |
| Loc 2 | TP 1 | 1.0m | 0.00000985 |
| Loc 2 | TP 2 | 0.5m | 0.00001037 |
| Loc 2 | TP 2 | 1.0m | 0.00000659 |
| Loc 3 | TP 1 | 0.5m | 0.00006427 |
| Loc 3 | TP 1 | 1.0m | 0.00003541 |
| Loc 3 | TP 2 | 0.5m | 0.00003715 |
| Loc 3 | TP 2 | 1.0m | 0.00002992 |

At Location 1, high permeability values reflect sandy or silty soils that drain quickly, resulting in faster consolidation and reduced risk of prolonged settlement. In Location 2, very low permeability is observed, typical of clay-dominated soils where water movement is impeded. This low permeability leads to slow consolidation, higher pore water pressure, and extended settlement times. Location 3 displays inconsistent permeability values, aligning with its mixed soil composition. Effective drainage systems are essential for low-permeability soils like those in Location 2 to enhance consolidation rates and reduce settlement periods.

3.1.6 Consolidation of Soil Samples

The consolidation results in table 7 gives information about soil settlement under sustained loading.

Table 7.	Consolidation of soil samples at different locations

| Location | Trial Pit | Depth | Coefficient of Consolidation (Cv) | Total settlement |
| --- | --- | --- | --- | --- |
| Loc 1 | TP 1 | 0.5m | 0.01216 | 1.1100 |
| Loc 1 | TP 1 | 1.0m | 0.00851 | 2.2700 |
| Loc 1 | TP 2 | 0.5m | 0.01174 | 1.5000 |
| Loc 1 | TP 2 | 1.0m | 0.01101 | 1.3800 |
| Loc 2 | TP 1 | 0.5m | 0.00928 | 1.6500 |
| Loc 2 | TP 1 | 1.0m | 0.00850 | 1.8900 |
| Loc 2 | TP 2 | 0.5m | 0.01024 | 2.2200 |
| Loc 2 | TP 2 | 1.0m | 0.00865 | 2.4600 |
| Loc 3 | TP 1 | 0.5m | 0.0187 | 1.2000 |
| Loc 3 | TP 1 | 1.0m | 0.01347 | 0.7500 |
| Loc 3 | TP 2 | 0.5m | 0.01212 | 1.0900 |
| Loc 3 | TP 2 | 1.0m | 0.01202 | 1.1100 |

Location 1 shows rapid consolidation due to its high permeability and low compressibility, making it ideal for time-sensitive construction projects. In Location 2, however, consolidation occurs slowly because of the low permeability and high void ratio, highlighting the need for preloading or vertical drains to accelerate settlement. Location 3 exhibits mixed consolidation behaviors due to its heterogeneous layers. These results reinforce the importance of consolidation analysis in predicting settlement behavior, particularly for clay-rich soils in Location 2 that may pose long-term risks to structural stability.

3.1.7 Correlational Analysis

Correlational analysis was carried out to determine the relationships between different soil parameters by the use of Minitab software. Table 8 presented results of correlation analysis between soil parameters, thus, showing their interrelationships. Figure 1 shows matrix plot visually complements the table 8 by illustrating scatter plots of parameter pairs, their correlation coefficients, and 95% confidence intervals.

Table 8.	Correlational Analysis between soil parameters

|  | OMC | C | O (phi) | UCS | TS | Cv | eo | e | K |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| OMC | 1 | 0.287 | -0.233 | 0.538 | -0.226 | 0.214 | -0.44 | 0.049 | -0.144 |
| C | 0.287 | 1 | -0.859 | -0.001 | -0.437 | 0.638 | -0.591 | -0.142 | -0.324 |
| O (phi) | -0.233 | -0.859 | 1 | 0.174 | 0.52 | -0.547 | 0.646 | -0.03 | 0.405 |
| UCS | 0.538 | -0.001 | 0.174 | 1 | 0.386 | -0.482 | -0.031 | 0.222 | 0.366 |
| TS | -0.226 | -0.437 | 0.52 | 0.386 | 1 | -0.677 | 0.692 | -0.386 | 0.907 |
| Cv | 0.214 | 0.638 | -0.547 | -0.482 | -0.677 | 1 | -0.516 | -0.351 | -0.621 |
| eo | -0.44 | -0.591 | 0.646 | -0.031 | 0.692 | -0.516 | 1 | -0.136 | 0.623 |
| e | 0.049 | -0.142 | -0.03 | 0.222 | -0.386 | -0.351 | -0.136 | 1 | -0.407 |
| K | -0.144 | -0.324 | 0.405 | 0.366 | 0.907 | -0.621 | 0.623 | -0.407 | 1 |

Fig. 1.	Matrix plot showing the correlation between soil parameters

A prominent observation is the strong negative correlation between cohesion (C) and the angle of shearing resistance (∅) with a coefficient of −0.859. This aligns with soil mechanics principles, as soils with higher cohesion typically exhibit lower shearing resistance due to their adhesive nature. Similarly, the negative relationship between the coefficient of consolidation (Cv) and total settlement (TS) (−0.677) suggests that soils with higher total settlement compress less during consolidation. Another notable inverse relationship is between coefficient of consolidation (Cv) and permeability (K), with a correlation of −0.621, indicating that soils with higher consolidation rates tend to have lower permeability. On the other hand, the table highlights strong positive correlations, such as the relationship between total settlement (TS) and permeability (K), which has a coefficient of 0.907. This implies that soils with greater total settlement are also more permeable, potentially due to their granular structure allowing water movement. Similarly, the correlation between the initial void ratio (eo) and total settlement (0.692) reflects that soils with higher void ratios exhibit higher settlement, likely due to their structural rearrangement during loading. A moderate positive correlation is also observed between optimum moisture content (OMC) and unconfined compressive strength (UCS) (0.538), indicating that soils with higher moisture content can achieve greater compressive strength. Interestingly, some parameters, such as Cohesion (C) and unconfined compressive strength (UCS), show negligible correlation (−0.001), suggesting they are largely independent of each other in the analyzed dataset.

The matrix plot (shown in Figure 1) visually complements the table by illustrating scatter plots of parameter pairs, their correlation coefficients, and 95% confidence intervals. Strong correlations, such as the negative relationship between cohesion (C) and the angle of shearing resistance (∅), are evident in the clear downward linear trend of scatter points. Positive correlations, like that between total settlement (TS) and permeability (K), are reflected in upward trends with tight clustering of points, signifying consistent relationships. Conversely, parameters with neutral correlations, such as cohesion (C) and unconfined compressive strength (UCS), display non-linear, scattered clustering, confirming the lack of significant interaction. Additionally, the variation in cluster density indicates the degree of variance within each relationship. Tighter clustering in total settlement (TS) vs. permeability (K) highlights a more consistent positive trend, while broader scatter in e vs. K reflects a weaker relationship. Beyond these, other notable interactions can be observed: cohesion (C) and UCS demonstrate a generally positive correlation, aligning with theoretical expectations that higher cohesion contributes to greater compressive strength. Similarly, UCS and tensile strength (TS) are positively related, suggesting soils stronger in compression also resist tensile stresses better. Void ratio (e, e₀) shows a clear negative relationship with strength parameters (C, UCS, and ∅), emphasizing that looser, more compressible soils tend to have lower shear and compressive resistance. A positive relationship between compression index (Cc) and void ratio (e) further supports the tendency of soils with larger initial voids to undergo greater compressibility. Finally, the coefficient of consolidation (Cv) and permeability (K) exhibit a strong positive correlation, reinforcing the principle that higher permeability leads to faster consolidation. These observed patterns collectively affirm that soil strength, compressibility, and drainage characteristics are interdependent, justifying the need for PCA and regression modeling to identify the most critical parameters influencing settlement behavior.

3.1.8 Principal Component Analysis

Table 9 shows the results of Principal Component Analysis (PCA) applied to geotechnical variables such as moisture content (MC), optimum moisture content (OMC), cohesion (C), angle of internal friction (∅), unconfined compressive strength (UCS), tensile strength (TS), coefficient of consolidation (Cv), void ratio (eo), settlement (e), hydraulic conductivity (K), maximum dry density (MDD), and shear strength (SS) using Minitab software. The table highlights the contributions of these variables to twelve principal components (PC1 to PC12), which are orthogonal and collectively explain the variability in the dataset. PCA is a valuable tool for dimensionality reduction and identifies underlying patterns among correlated variables.

Table 9.	Principal Component Analysis: MC, OMC, C, ∅, UCS, TS, Cv, eo, e, K, MDD, SS

| Variable | PC1 | PC2 | PC3 | PC4 | PC5 | PC6 | PC7 | PC8 | PC9 | PC10 | PC11 | PC12 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| MC | -0.201 | -0.454 | 0.124 | -0.210 | -0.452 | -0.258 | 0.212 | -0.184 | 0.309 | -0.456 | -0.196 | -0.056 |
| OMC | -0.229 | -0.472 | -0.056 | -0.025 | 0.169 | 0.392 | -0.568 | 0.387 | 0.140 | -0.174 | 0.086 | -0.097 |
| C | -0.322 | 0.058 | 0.254 | 0.371 | 0.500 | -0.179 | 0.210 | 0.074 | -0.157 | -0.298 | -0.226 | -0.440 |
| ∅ | 0.353 | -0.142 | -0.128 | -0.463 | 0.034 | -0.105 | 0.031 | 0.065 | -0.089 | 0.211 | -0.002 | -0.744 |
| UCS | 0.060 | -0.506 | -0.206 | 0.318 | 0.317 | -0.285 | -0.041 | -0.353 | 0.263 | 0.453 | -0.091 | 0.081 |
| TS | 0.359 | -0.196 | 0.253 | 0.267 | -0.089 | -0.001 | -0.250 | -0.426 | -0.375 | -0.307 | 0.448 | -0.098 |
| Cv | -0.332 | 0.149 | 0.336 | -0.321 | 0.258 | 0.058 | 0.074 | -0.280 | 0.396 | 0.130 | 0.565 | -0.074 |
| eo | 0.383 | 0.072 | 0.074 | -0.024 | 0.224 | 0.612 | 0.126 | -0.337 | 0.320 | -0.199 | -0.381 | -0.024 |
| e | -0.045 | 0.057 | -0.763 | 0.141 | 0.069 | 0.078 | 0.298 | -0.037 | 0.112 | -0.347 | 0.385 | -0.101 |
| K | 0.317 | -0.221 | 0.303 | 0.329 | -0.128 | 0.120 | 0.462 | 0.500 | 0.245 | 0.131 | 0.281 | -0.018 |
| MDD | 0.296 | 0.386 | 0.008 | 0.179 | -0.030 | -0.411 | -0.434 | 0.135 | 0.548 | -0.200 | -0.006 | -0.118 |
| SS | 0.315 | -0.158 | 0.036 | -0.408 | 0.518 | -0.296 | 0.107 | 0.200 | -0.102 | -0.307 | 0.052 | 0.439 |

Table 9 highlights the contributions of these variables to twelve principal components (PC1 to PC12), which are orthogonal and collectively explain the variability in the dataset. PCA is a valuable tool for dimensionality reduction and identifies underlying patterns among correlated variables.

Each variable is represented by a set of loadings, which indicate its influence on each principal component. From the results, PC1 has high positive loadings for void ratio (eo), hydraulic conductivity (K), and shear strength (SS), indicating that these variables are strongly correlated and likely contribute significantly to the variability in soil behavior captured by this component. Similarly, PC2 shows notable loadings for MC (-0.454), OMC (-0.472), and UCS (-0.506), which may reflect the interconnected role of moisture properties and soil strength characteristics. PC3 is dominated by void-related variables, as shown by its large negative loading for settlement (e, -0.763). This emphasizes the relationship between settlement behavior and soil structure, as indicated by the void ratio. In PC4, cohesion (C) and the angle of internal friction (∅) show significant contrasting effects. While cohesion has a high positive loading (0.371), ∅ is negatively loaded (-0.463), revealing their inversely proportional influence in this component. Other notable patterns include the relatively high positive loadings for tensile strength (TS) in PC6, and the strong influence of Maximum Dry Density (MDD) in PC9. These trends suggest the principal components distinctly capture aspects of compaction, strength, permeability, and soil structure. Some variables, such as MC, OMC, and UCS, consistently exhibit large negative loadings across multiple principal components, highlighting their importance in influencing various geotechnical characteristics. The moderate loadings of hydraulic conductivity (K) and cohesion (C) across several components show their balanced contribution to variability in the dataset.

The PCA results reveal that soil behavior is governed by the interplay between different groups of variables that can be summarized in fewer dimensions. PC1 predominantly relates to soil compaction and strength properties, as seen in variables like void ratio and hydraulic conductivity, which define soil’s load-bearing capabilities and permeability. PC2 captures the influence of moisture-related properties like MC and OMC, alongside strength parameters such as UCS, highlighting the close link between moisture conditions and soil strength.

The outcomes suggest that soil engineering properties are highly interdependent, and PCA has effectively identified the dominant factors influencing these properties. This highlights the importance of focusing on a few critical variables, such as cohesion, hydraulic conductivity, void ratio, and UCS, when designing geotechnical solutions. Furthermore, the PCA has confirmed that variables like MDD and TS are central to soil strength and compaction characteristics. The analysis supports the interpretation of soil behavior and facilitates the reduction of complexity in studying soil properties, thus aiding in efficient modeling and decision-making in geotechnical engineering.

The first principal component (PC1) is strongly associated with void ratio (eo), hydraulic conductivity (K), and shear strength (SS). This suggests that PC1 primarily captures the balance between soil structure and permeability, a well-documented trade-off in soil mechanics. Soils with a higher void ratio typically exhibit greater hydraulic conductivity but lower strength, since increased pore space allows easier flow of water while reducing inter-particle friction. This is consistent with classical consolidation theory, where compressible soils with higher void ratios are also more susceptible to settlement under loading. PC2, on the other hand, shows strong negative loadings for UCS and OMC, indicating that this component reflects the strength–moisture interaction. In practical terms, soils at higher moisture contents often display reduced unconfined compressive strength because excess pore water weakens inter-particle bonds. This aligns with the observed laboratory results where wetter samples produced lower strength values

These findings also align with earlier research that highlighted the competing influence of density, void structure, and permeability on soft soil behavior. For example, Dolinar (2009) and Su et al., (2020) emphasized that void ratio and hydraulic conductivity often dominate the variability in soft clay deposits, while other studies reported that compressive strength and consolidation parameters are primarily moisture-dependent (Ackah et al., 2022; Ma et al., 2023; Onyelowe et al., 2023; Shimbo et al., 2022; Wang et al., 2022). The PCA in this study therefore confirms these trends, but with a novel contribution in showing that tensile strength (TS) and shear strength (SS) also load significantly on the first two components, suggesting they are co-dependent with permeability and compaction behavior in the studied soils. The PCA demonstrates that soil settlement behavior is controlled by two dominant mechanisms: (i) the structural framework of the soil (void ratio, permeability, shear strength), and (ii) the moisture–strength relationship (UCS, OMC, MC). This provides a more intuitive understanding of the complex multivariate dataset, highlighting that both structural and hydraulic parameters must be considered together when predicting soft soil settlement.

3.2 Regression Analysis

Table 10 presented the regression models developed for the geotechnical properties of the soil samples using Minitab software. Table 11 to Table 14 provided the residual values between the measured and predicted total settlement, unconfined compressive strength, shear strength and permeability values respectively at various depths across different trial pits and locations. Figure 2 to 9 gives the residual vs fitted plot and Q-Q plot for the regression models. The parameters considered in the regression analysis are moisture content, compaction parameters, void ratio, compression index, cohesion and friction angle, and unconfined compression strength. These parameters are considered for their mechanistic influence on settlement. Higher moisture increases void ratio and reduces effective stress, contributing to greater compressibility Void ratio directly governs compressibility, with higher e leading to higher settlements under loading. Compression index defines the slope of the virgin compression curve, making it a primary settlement predictor. Cohesion and friction angle influence shear resistance, indirectly affecting load-carrying capacity and deformation. And unconsolidated compressive strength provides undrained strength, which, when low, indicates susceptibility to large settlements under applied loads.

Table 10.	Regression model equation for the soil samples

| S/N | Model Equation | R2 (%) |
| --- | --- | --- |
| 1. | TS = 0.241 - 0.000498 MC - 0.001422 OMC - 0.000119 MDD - 0.000234 C + 0.000227 ∅ + 271.3 K | 98.72 |
| 2. | UCS = -1427 + 0.87 MC + 14.92 OMC + 0.688 MDD + 1.624 C + 0.324 ∅ - 476093 K | 97.02 |
| 3. | SS = 318.1 + 4.717 MC - 19.68 OMC - 0.1179 MDD + 2.633 UCS - 2759265 K + 15547 TS | 99.87 |
| 4. | K = -0.001651 + 0.000004 MC + 0.000010 OMC + 0.000001 MDD + 0.000001 C - 0.000001 ∅ + 0.000618 eo | 98.01 |

Table 11.	Residual Values Between Predicted Values and Measured Values of Total Settlement

| Location | Trial Pit | Depth | Sample ID | Measured | Predicted | Residuals |
| --- | --- | --- | --- | --- | --- | --- |
| Loc 1 | TP 1 | 0.5m | 1 | 0.01216 | 0.0120462 | 0.0001138 |
| Loc 1 | TP 1 | 1.0m | 2 | 0.00851 | -0.0140624 | 0.0225724 |
| Loc 1 | TP 2 | 0.5m | 3 | 0.01174 | -0.0060639 | 0.0178039 |
| Loc 1 | TP 2 | 1.0m | 4 | 0.01101 | 0.0040338 | 0.0069762 |
| Loc 2 | TP 1 | 0.5m | 5 | 0.00928 | 0.0137127 | -0.0044327 |
| Loc 2 | TP 1 | 1.0m | 6 | 0.00850 | 0.0088023 | -0.0003023 |
| Loc 2 | TP 2 | 0.5m | 7 | 0.01024 | 0.0106405 | -0.0004005 |
| Loc 2 | TP 2 | 1.0m | 8 | 0.00865 | 0.0080467 | 0.0006033 |
| Loc 3 | TP 1 | 0.5m | 9 | 0.01870 | 0.0185557 | 0.0001443 |
| Loc 3 | TP 1 | 1.0m | 10 | 0.01347 | 0.0132828 | 0.0001872 |
| Loc 3 | TP 2 | 0.5m | 11 | 0.01212 | 0.0126106 | -0.0004906 |
| Loc 3 | TP 2 | 1.0m | 12 | 0.01202 | 0.0118750 | 0.0001450 |

Fig. 2. Residuals vs Fitted Plot for 		Fig. 3. Q-Q Plot for Total Settlement

Total Settlement				Model

Table 12.	Residual Values Between Predicted Values and Measured Values of Unconfined Compressive Strength

| Location | Trial Pit | Depth | Sample ID | Measured | Predicted | Residuals |
| --- | --- | --- | --- | --- | --- | --- |
| Loc 1 | TP 1 | 0.5m | 1 | 45.2 | 45.839 | -0.639 |
| Loc 1 | TP 1 | 1.0m | 2 | 35.0 | 172.258 | -137.258 |
| Loc 1 | TP 2 | 0.5m | 3 | 34.5 | 85.518 | -51.018 |
| Loc 1 | TP 2 | 1.0m | 4 | 39.5 | 51.467 | -11.967 |
| Loc 2 | TP 1 | 0.5m | 5 | 25.0 | 7.1906 | 17.8094 |
| Loc 2 | TP 1 | 1.0m | 6 | 25.0 | 23.3023 | 1.6977 |
| Loc 2 | TP 2 | 0.5m | 7 | 49.7 | 47.4506 | 2.2494 |
| Loc 2 | TP 2 | 1.0m | 8 | 29.8 | 33.1878 | -3.3878 |
| Loc 3 | TP 1 | 0.5m | 9 | 39.5 | 40.3104 | -0.81041 |
| Loc 3 | TP 1 | 1.0m | 10 | 44.2 | 45.2511 | -1.05112 |
| Loc 3 | TP 2 | 0.5m | 11 | 49.1 | 46.3446 | 2.75545 |
| Loc 3 | TP 2 | 1.0m | 12 | 63.1 | 63.9142 | -0.81420 |

Fig. 4. Residuals vs Fitted Plot for 		Fig. 5. Q-Q Plot for Unconfined

Unconfined Compressive Strength (UCS) 	Compressive Strength (UCS) Model

Model

Table 13.	Residual Values Between Predicted Values and Measured Values of Shear Strength

| Location | Trial Pit | Depth | Sample ID | Measured | Predicted | Residuals |
| --- | --- | --- | --- | --- | --- | --- |
| Loc 1 | TP 1 | 0.5m | 1 | 150.309 | 150.530 | -0.222 |
| Loc 1 | TP 1 | 1.0m | 2 | 119.890 | 74.722 | 45.168 |
| Loc 1 | TP 2 | 0.5m | 3 | 96.411 | 220.737 | -124.326 |
| Loc 1 | TP 2 | 1.0m | 4 | 147.244 | 222.268 | -75.024 |
| Loc 2 | TP 1 | 0.5m | 5 | 126.862 | 114.370 | 12.4917 |
| Loc 2 | TP 1 | 1.0m | 6 | 148.402 | 149.076 | -0.6739 |
| Loc 2 | TP 2 | 0.5m | 7 | 159.627 | 160.792 | -1.1642 |
| Loc 2 | TP 2 | 1.0m | 8 | 108.523 | 107.179 | 1.3441 |
| Loc 3 | TP 1 | 0.5m | 9 | 177.257 | 177.470 | -0.21296 |
| Loc 3 | TP 1 | 1.0m | 10 | 175.257 | 174.117 | 1.14031 |
| Loc 3 | TP 2 | 0.5m | 11 | 102.146 | 103.292 | -1.14546 |
| Loc 3 | TP 2 | 1.0m | 12 | 145.005 | 144.071 | 0.93403 |

Fig. 6. Residuals vs Fitted Plot 			Fig. 7. Q-Q Plot for Shear Strength

for Shear Strength				Model

Table 14.	Residual Values Between Predicted Values and Measured Values of Permeability

| Location | Trial Pit | Depth | Sample ID | Measured | Predicted | Residuals |
| --- | --- | --- | --- | --- | --- | --- |
| Loc 1 | TP 1 | 0.5m | 1 | 0.0000101 | 0.0000098 | 0.0000003 |
| Loc 1 | TP 1 | 1.0m | 2 | 0.0000090 | 0.0001258 | -0.0001168 |
| Loc 1 | TP 2 | 0.5m | 3 | 0.0000148 | 0.0000795 | -0.0000647 |
| Loc 1 | TP 2 | 1.0m | 4 | 0.0000129 | 0.0000355 | -0.0000226 |
| Loc 2 | TP 1 | 0.5m | 5 | 0.0000121 | -0.0000202 | 0.0000322 |
| Loc 2 | TP 1 | 1.0m | 6 | 0.0000099 | 0.0000089 | 0.0000010 |
| Loc 2 | TP 2 | 0.5m | 7 | 0.0000104 | 0.0000071 | 0.0000032 |
| Loc 2 | TP 2 | 1.0m | 8 | 0.0000066 | 0.0000101 | -0.0000035 |
| Loc 3 | TP 1 | 0.5m | 9 | 0.0000643 | 0.0000626 | 0.0000017 |
| Loc 3 | TP 1 | 1.0m | 10 | 0.0000354 | 0.0000388 | -0.0000034 |
| Loc 3 | TP 2 | 0.5m | 11 | 0.0000372 | 0.0000338 | 0.0000034 |
| Loc 3 | TP 2 | 1.0m | 12 | 0.0000299 | 0.0000326 | -0.0000027 |

Fig. 8  Residuals vs Fitted Plot for	 	Fig. 9. Q-Q Plot for Shear Strength

Permeability Model				Model

Various regression models were developed for key properties such as total settlement (TS), unconfined compressive strength (UCS), and permeability (K). The models show the relationships between geotechnical properties and the independent variables considered. The total settlement (TS) model achieved an R² value of 98.72%, indicating a strong correlation between the independent variables and TS. Similarly, the unconfined compressive strength (UCS) model exhibited an R² of 97.02%, demonstrating its reliability. The shear strength (SS) model, with an R² of 99.87%, was highly accurate, while the permeability (K) model had an R² of 98.01%, suggesting a good fit. These models account for multiple variables, including moisture content (MC), optimum moisture content (OMC), maximum dry density (MDD), cohesion (C), angle of internal friction (∅), and void ratio (eo).

Residual values between measured and predicted total settlements were computed to assess model accuracy. Most residuals were minimal, signifying the models' reliability, although a few discrepancies suggest potential variances in soil heterogeneity or experimental conditions. Table 12 to Table 14 provides the residual values between the measured and predicted total settlement, unconfined compressive strength, shear strength, and permeability values respectively at various depths across different trial pits and locations. The residuals observed were generally minimal, with some discrepancies noted. Notably, a few large residuals were observed (e.g., UCS: −137.258 kPa at Loc. 1, TP 1, 1.0 m; Shear Strength: −124.326 kN/m² at Loc. 1, TP 2, 0.5 m). These discrepancies may be attributed to experimental variability during testing, soil heterogeneity and anisotropy within the samples, or limitations of the regression framework in capturing highly non-linear behaviour. While these instances do not invalidate the models, they highlight the importance of further validation using independent datasets and potentially more advanced testing (e.g., triaxial or stress-path dependent experiments) to enhance robustness. Incorporating a larger sample size and microstructural characterization could also reduce unexplained variability and improve predictive accuracy.

The regression models developed in this study achieved exceptionally high coefficients of determination (R² values above 97% across all property models), indicating a strong predictive capacity. This performance aligns with, yet in some cases surpasses, earlier works that have employed regression approaches for geotechnical property estimation

Thus, while the high overall fits demonstrate robustness, the presence of notable residuals reinforces existing cautions in the literature about over-reliance on empirical models without complementary mechanistic or constitutive modeling (Ozil, 2022). The regression models were designed as empirical correlations to explore relationships among measured soil properties. While empirical models lack the rigorous physical basis of constitutive soil mechanics models, they serve as practical tools for preliminary settlement prediction. To strengthen the geotechnical relevance, model variables were selected based on established soil mechanics principles (e.g., settlement dependence on compressibility, void ratio, and moisture content). This provides a physical rationale for the inclusion of predictors, even though the models themselves remain empirical.

3.3 Contribution to Knowledge

The novelty in this research lies in its application of Principal Component Analysis (PCA) to comprehensively analyze and reduce the dimensionality of multiple geotechnical properties of soils. The novelty of this study does not lie in the use of these routine tests, but rather in the integration of experimental data with advanced statistical modeling techniques to enhance settlement prediction. While many studies have examined soil behavior using direct relationships between individual properties, this research provides a holistic approach by statistically identifying the dominant factors influencing the interplay among multiple soil parameters, such as moisture properties, strength characteristics, compaction metrics, and hydraulic conductivity. The innovative aspect is the integration of PCA as a data-driven tool to systematically unravel the complexity of interdependencies within the geotechnical dataset, enabling a more refined understanding of soil behavior. Specifically, this study is among the first to combine Principal Component Analysis (PCA) with regression modeling to identify the dominant factors influencing soft soil settlement and to develop a predictive framework. While PCA has been applied in soil science, its application in conjunction with regression to systematically quantify settlement behavior in highly plastic soft clays is rare in existing literature.

Another unique feature of this research is the identification of clusters of variables (e.g., moisture-related, strength-related, and structure-related properties) and their specific roles in influencing soil performance. By linking PCA-derived principal components to geotechnical behavior, the study not only reduces the number of variables required for predictive modeling but also introduces a systematic framework for evaluating soil parameters beyond conventional methods. The coupling of PCA with geotechnical engineering signifies a methodological shift from traditional experimental analysis to a statistically driven, big-picture perspective of soil mechanics.

3.4 Experimental Limitations

While the study provides valuable insights into the behavior of soft soils across the three locations and two trial pits investigated, it is important to acknowledge certain limitations. The sample size, although adequate for exploratory analysis, may not fully represent the regional variability of soft soils in southwestern Nigeria. Soils are inherently heterogeneous, and differences in depositional history, groundwater conditions, and mineralogical composition may lead to variations that were not fully captured in this study. The results are applicable primarily to the studied soils, while also serving as a foundation for future multi-site studies with greater geographical diversity. Future research should therefore extend the sampling framework to include a broader geographical spread and deeper profiles to improve the robustness of the conclusions and enhance their applicability to regional geotechnical practice.

The measured hydraulic conductivity values, ranging between 10⁻⁵ and 10⁻⁶ cm/s, fall within the expected range for fine-grained clays, indicating relatively low permeability. When compared with other soft soils reported in Nigeria and similar tropical regions, these results are consistent. For instance, studies on Lagos marine clays and coastal deposits in the Niger Delta report hydraulic conductivity values typically in the order of 10⁻⁶–10⁻⁷ cm/s, reflecting similarly low drainage potential and high compressibility. This contextual comparison suggests that the soils examined in this study behave in line with regional trends, reinforcing their classification as problematic soft soils with significant settlement potential under loading.

In this study, direct shear and unconfined compressive strength (UCS) tests were employed to evaluate the shear strength parameters of the soft soils. While these conventional tests provide valuable first-order approximations, they do not capture the full stress-path dependent behavior of soils. Advanced testing, particularly consolidated undrained (CU) triaxial tests with pore pressure measurements, are recognized as more rigorous methods for characterizing soft clay behavior under varied loading paths. Due to equipment and logistical constraints, triaxial testing was not conducted in this study. Instead, the focus was on widely adopted standard tests to establish baseline correlations. Future investigations should incorporate triaxial and stress-path controlled laboratory testing to enhance the predictive framework and ensure more robust generalisability of results.

Microstructural analysis such as scanning electron microscopy (SEM), X-ray diffraction (XRD), and energy dispersive spectroscopy (EDS) was not performed in the present study. Thus it is recommended that SEM/XRD/EDS and pore-size (MIP) analysis be carried out in future work to link fabric and mineralogy to mechanical behaviour.

The present study is based on laboratory-scale tests on limited soil volumes. Scale effects were not explicitly addressed, and no Representative Elementary Volume (REV) analysis was performed. This omission may affect the transferability of micro-scale measurements (e.g., void ratio, UCS) to field-scale settlement predictions. Future work should include REV analysis to establish the appropriate scale of testing for reliable upscaling

3.5 Predictive Framework Limitations

The regression and PCA-based predictive framework developed in this study demonstrated strong statistical performance, with R² values exceeding 97% for key soil properties. However, it must be emphasized that the models are empirical in nature and are best interpreted as first-level predictive tools applicable to similar geological and geotechnical conditions. Their generalisability is constrained by the limited sampling area and depth, as well as the absence of advanced stress-path dependent testing. Future research should validate these models with a more geographically diverse dataset, incorporate deeper sampling profiles, and integrate advanced constitutive models or numerical simulations to enhance robustness and reliability.

During regression analysis, multicollinearity among predictors was identified as a potential limitation, particularly between parameters such as void ratio and moisture content. To mitigate this, principal component analysis (PCA) was applied to identify dominant, non-redundant variables. However, the presence of correlated predictors may still influence coefficient stability. Future refinements will employ variance inflation factor (VIF) diagnostics or ridge regression to better handle multicollinearity.

A limitation of this study is that the regression models were developed and tested using the same dataset. Independent validation against a separate dataset was not feasible within the current scope. To ensure generalisability, future work will test the models on additional sites and datasets, thereby confirming predictive reliability across different geological settings.

While most residuals were small, some outliers (e.g., UCS and shear strength at Loc 1, TP 2) showed large discrepancies between measured and predicted values. These may arise from soil heterogeneity, experimental variability, or model limitations. Such deviations suggest the regression framework alone cannot fully capture soil behavior, reinforcing the need for advanced modeling approaches (e.g., constitutive models or machine learning techniques). Additional validation on larger datasets will help resolve these issues.

4. Conclusion

This study highlights the importance of characterizing soft soils to better understand their settlement behavior under loading. The analysis revealed that soils at Location 2, particularly the highly plastic and compressible clays, present significant challenges that necessitate stabilization before construction. Appropriate methods include chemical stabilization (lime, cement, fly ash), preloading with vertical drains, and the use of geosynthetics or stone columns to improve strength and reduce compressibility.

The correlation analysis confirmed several soil mechanics principles, such as the inverse relationship between cohesion and angle of shearing resistance, and the positive association between void ratio, compressibility, and settlement. These interdependencies emphasize that settlement is controlled by a combination of strength, compressibility, and drainage characteristics. The PCA further identified the most influential parameters, offering a systematic approach for prioritizing factors in soft soil performance.

Regression models developed in this study achieved high R² values, indicating strong site-specific predictive capacity. However, the residuals highlighted notable discrepancies in some parameters, suggesting that while the models are useful design aids, they should not be treated as universally generalisable. Instead, they must be validated with independent datasets and, where possible, supported by advanced testing such as triaxial shear or stress-path analysis.

Overall, this research contributes a structured framework for linking geotechnical parameters with settlement behavior, but it also reinforces the need for cautious application of empirical models. Future studies should extend the sampling depth, incorporate broader geological settings, and investigate time-dependent settlement to enhance predictive reliability.

References

Ackah, F. S., Hailiang, W., Huaiping, F., Cheng, L., & Feng, L. Z. (2022). Use of Taguchi method to evaluate the unconfined compressive strength of quicklime stabilized silty clayey subgrade. Case Studies in Construction Materials, 17, e01417.

Amadi, A. I. (2022). Construction Resources Management in Niger Delta's Coastal Environments: Hydro-Geomorphological Challenges to Sustainability. *Journal of Offshore Structure and Technology*, *9*(2), 28-33. https://doi.org/10.37591/JOOST.V9I2.1600

Chen, W., Ding, J., Wang, T., Connolly, D. P., & Wan, X. (2023). Soil property recovery from incomplete in-situ geotechnical test data using a hybrid deep generative framework. Engineering Geology, 326, 107332. https://doi.org/10.1016/j.enggeo.2023.107332

Demattê, J. A. M., Dotto, A. C., Bedin, L. G., Sayão, V. M., & Souza, A. B. E. (2019). Soil analytical quality control by traditional and spectroscopy techniques: Constructing the future of a hybrid laboratory for low environmental impact. Geoderma, 337, 111-121. https://doi.org/10.1016/j.geoderma.2018.09.010

Díaz-Rodríguez, J. A., & González-Rodríguez, R. (2013). Influence of diatom microfossils on soil compressibility. In Proceedings of the 18th international conference on soil mechanics and geotechnical engineering, Paris, France (pp. 2-5).

Dolinar, B. (2009). Predicting the hydraulic conductivity of saturated clays using plasticity-value correlations. Applied Clay Science, 45(1-2), 90-94. https://doi.org/10.1016/j.clay.2009.04.001

Feng, Qiao., Jingshan, Bo., WenHao, Qi., Liang, Wang., chaoyu, chang., Zhaopeng, Zhang., Jing, Wang. (2020). Study on the dynamic characteristics of soft soil. RSC Advances, 10(8):4630-4639. doi: 10.1039/C9RA05700E

Gue, S. S., & Gue, C. S. (2022). Geotechnical challenges on soft ground. Journal of Civil Engineering, Science and Technology, 13(2), 84–96. https://doi.org/10.33736/jcest.4760.2022

Harshit, V., & Abhivek, S. (2024). A study on the behaviour of soft clay under embankment loading. In IOP Conference Series: Earth and Environmental Science (Vol. 1326, No. 1, p. 012120). IOP Publishing.

Lin, P., Chen, X., Jiang, M., Song, X., Xu, M., & Huang, S. (2022). Mapping shear strength and compressibility of soft soils with artificial neural networks. Engineering Geology, 300, 106585. https://doi.org/10.1016/j.enggeo.2022.106585

Liu, S. J., Geng, X. Y., Sun, H. L., Cai, Y. Q., Pan, X. D., & Shi, L. (2019). Nonlinear consolidation of vertical drains with coupled radial‐vertical flow considering time and depth dependent vacuum pressure. International Journal for Numerical and Analytical Methods in Geomechanics, 43(4), 767-780. https://doi.org/10.1002/nag.2888

Ma, S., Yao, Y., Bao, P., & Guo, C. (2023). Effects of moisture content on strength and compression properties of foundation soils of cultural relics in areas flooded by the Yellow River. Frontiers in Materials, 10, 1186750. https://doi.org/10.3389/fmats.2023.1186750

Mbevo Fendoung, P., & Hubert-Ferrari, A. (2025). Hydrogeomorphological dynamics and erosion of the soft coasts in tropical Africa, the case study of the Wouri estuary, Cameroon. Discover Geoscience, 3, 48. https://doi.org/10.1007/s44288-025-00154-1

Mohamad, N. O., Razali, C. E., Hadi, A. A. A., Som, P. P., Eng, B. C., Rusli, M. B., & Mohamad, F. R. (2016). Challenges in Construction Over Soft Soil - Case Studies in Malaysia. IOP Conference Series: Materials Science and Engineering, 136, 012002. https://doi.org/10.1088/1757-899X/136/1/012002

Nguyen, N. T. (2024). Long-Term Settlement Prediction for Over- Consolidated Soft Clay under Low Embankment. Engineering, Technology & Applied Science Research, 14(6), 18592–18599. https://doi.org/10.48084/etasr.9211

O'Kelly, B. C., & Pichan, S. P. (2013). Effects of decomposition on the compressibility of fibrous peat — A review. Geomechanics and Geoengineering: An International Journal, 9(4), 286–296. https://doi.org/10.1080/17486025.2013.804210

Onyelowe, K. C., Ebid, A. M., Sujatha, E. R., Fazel-Mojtahedi, F., Golaghaei-Darzi, A., Kontoni, D. N., & Nooralddin-Othman, N. (2023). Extensive overview of soil constitutive relations and applications for geotechnical engineering problems. Heliyon, 9(3), e14465. https://doi.org/10.1016/j.heliyon.2023.e14465

Shimbo, T., Shinzo, C., Uchii, U., Itto, R., & Fukumoto, Y. (2022). Effect of water contents and initial crack lengths on mechanical properties and failure modes of pre-cracked compacted clay under uniaxial compression. Engineering Geology, 301, 106593. https://doi.org/10.1016/j.enggeo.2022.106593

Su, W., Cui, Y., Zhang, F., & Ye, W. (2020). Revisiting the methods of determining hydraulic conductivity of saturated expansive clays in low-compressibility zone. Journal of Rock Mechanics and Geotechnical Engineering, 12(5), 1131-1136. https://doi.org/10.1016/j.jrmge.2020.01.004

Ural, N. (2018). The Importance of Clay in Geotechnical Engineering. InTechOpen. https://doi.org/10.5772/intechopen.75817

Varghese, R., Chandrakaran, S., & Rangaswamy, K. (2021). Influence of type of organic substances on the strength and consolidation behaviour of inorganic clay soil. International Journal of Geotechnical Engineering. https://doi.org/10.1080/19386362.2019.1600000

Wang, C., Li, Z., Cai, B., Tan, Q., Li, Y., He, L., ... Deng, Y. (2022). Effect of root system of the Dicranopteris dichotoma on the soil unconfined compressive strength of collapsing walls in hilly granite area of South China. *Catena*, *216*, 106411. https://doi.org/10.1016/j.catena.2022.106411

Wang, J., Xie, Y., Guo, T., & Du, Z. (2023). Predicting the Influence of Soil–Structure Interaction on Seismic Responses of Reinforced Concrete Frame Buildings Using Convolutional Neural Network. Buildings, 13(2), 564. https://doi.org/10.3390/buildings13020564

Xiao, J., Wang, B., Wei, R., Wu, S., & Cai, H. (2021). Study on the geometry and spatial distribution characteristics of physical and mechanical indexes of soft clay. IOP Conference Series: Earth and Environmental Science, 861(4), 042094. https://doi.org/10.1088/1755-1315/861/4/042094

Zhou, H., Zhang, J., Yu, X., Hu, Q., Zheng, G., Xu, H., Shi, Y., He, Y., & Yang, S. (2024). Stochastic Bearing Capacity and Failure Mechanism of Footings Placed Adjacent to Slopes considering the Anisotropic Spatial Variability of the Clay Undrained Strength. International Journal of Geomechanics https://doi.org/10.1061/(ASCE)GM.1943-5622.0003090

Ozili, P. K. (2022). The Acceptable R-Square in Empirical Modelling for Social Science Research. SSRN Electronic Journal. https://doi.org/10.2139/ssrn.4128165.