Zingiber officinale (ginger) extract as a green biocide for the inhibition of copper corrosion by Pseudomonas species

ABSTRACT

This study investigates Zingiber officinale (ginger) extract as a sustainable corrosion inhibitor and antimicrobial agent for copper in a microbiologically active environment containing Pseudomonas aeruginosa. Copper coupons (2.0 × 2.0 × 0.14 cm) were exposed to microbiologically active conditions with and without ginger extract. Phytochemical constituents were identified, and corrosion behaviour was evaluated using weight loss measurements, potentiodynamic polarization (PDP), and electrochemical impedance spectroscopy (EIS). Antimicrobial activity against P. aeruginosa was assessed via the agar disc diffusion method. Phytochemical analysis confirmed the presence of corrosion-inhibitive bioactive compounds, including gingerol, shogaol, and fatty acids. Copper corrosion was significantly suppressed by the adsorption of extract constituents onto the metal surface. While corrosion rate and weight loss increased with exposure time, both were markedly reduced in the inhibited system. PDP analysis showed that corrosion rate and corrosion current density increased from 2.112 mpy and 4.620 µA cm⁻² in the sterile system to 2.620 mpy and 5.730 µA cm⁻² in the presence of P. aeruginosa. EIS results revealed a pronounced increase in polarization resistance from 98.61 Ω (uninhibited) to 3.15 × 10⁴ Ω with ginger extract. Zingiber officinale extract exhibits strong dual-function performance as a green corrosion inhibitor and antimicrobial agent for copper, offering effective protection in microbiologically influenced corrosion environments.

Keywords: Microbial corrosion, copper, green biocide, inhibition, corrosion rate, sustainable corrosion mitigation

- INTRODUCTION

Corrosion of metals, including copper, poses significant economic and environmental challenges across various industries worldwide, (Wanget et al 2020). Corrosion, the gradual degradation of materials through chemical or electrochemical reactions with their environment, poses significant challenges across various industries, including infrastructure, transportation, and manufacturing (Fontana 2005). Among the diverse forms of corrosion, microbial corrosion, or microbiologically influenced corrosion (MIC), has gained prominence due to its detrimental effects on metal structures and components.

Among the multitude of factors contributing to corrosion, microbial activity, particularly by species such as Pseudomonas, has emerged as a major concern (Beech & Sunner 2004). Pseudomonas spp. is notorious for their ability to form biofilms on metal surfaces, leading to accelerated corrosion rates through mechanisms such as biofilm-induced localized corrosion and production of corrosive metabolic byproducts (Videla & Herrera 2005). Traditional methods of corrosion control often rely on the use of chemical biocides, which may pose environmental risks due to their toxicity and persistence in ecosystems Shi et al 2023. Hence, there is a growing interest in exploring natural, eco-friendly alternatives for corrosion inhibition. Ginger (Zingiber officinale), a widely used spice and medicinal plant, has gained attention for its potent antimicrobial properties attributed to bioactive compounds such as gingerol and zingerone (Prasad & Tyagi 2015). Previous studies have demonstrated the antimicrobial efficacy of ginger extracts against a range of bacterial strains, including Pseudomonas species (Kasi et al 2024). However, the application of ginger as a green biocide for inhibiting Pseudomonas corrosion of copper remains relatively unexplored. This gap in knowledge underscores the need for systematic investigation to evaluate the potential of ginger extracts as corrosion inhibitors in industrial settings. Microbially influenced corrosion (MIC) is a destructive type of corrosion that is initiated, facilitated, or accelerated by the presence and metabolic activity of bacteria and mostly appear in the form of localized pits and crevices on metal surfaces (Eyu et al 2013; Oguzie et al 2012; Imo et al 2023). MIC of metals is a great issue in many industries such as marine, freshwater systems, and gas/oil pipelines. Bacteria tend to attach to a substrate and form a biofilm layer where it creates an environment suitable for the acceleration of corrosion. The bacteria in the biofilm state tend to accelerate and facilitate the corrosion and cause severe damage to the metals (Avelino-Jiménez et al 2023). Biofilms play a crucial role in microbial corrosion by providing a protective environment for bacteria to thrive on metal surfaces. Pseudomonas species are adept at forming biofilms through a combination of adhesion, aggregation, and extracellular matrix production (Flemming et al 2016). These biofilms create microenvironments where bacteria can concentrate, facilitating the accumulation of corrosive metabolites and creating localized anaerobic conditions conducive to corrosion (Dang & Lovell 2016). Pseudomonas species is known for its diverse metabolic capabilities, which contribute to corrosion processes. These bacteria can metabolize a wide range of organic and inorganic compounds present in their environment, producing corrosive byproducts such as organic acids, hydrogen sulfide, and other sulfur compounds (Videla & Herrera 2005). The production of corrosive metabolites by Pseudomonas species can accelerate the degradation of metal surfaces, leading to localized pitting corrosion and material loss (Beech & Sunner 2004; Nwokorie et al 2025). This study provides valuable insight into the potential use of ginger extracts and ginger-derived compounds such as green biocides and corrosion inhibitors.

2.0 MATERIAL AND METHODS

Metal coupons: The copper used in this study was obtained from the material and metallurgical department of the University. The copper was first cut into coupons of specific dimension 2cm x 2cm x 0.14 cm. Thereafter the coupons were polished with silicon carbide abrasive paper (from grade no. 400 to 1000), then cleaned with distilled water, dried in acetone and weighed with electronic weighing balance (Nicolet Model 37500).

Weighed coupons were stored in moisture-free desiccators prior to use.

Isolation and identification:

The strain of Pseudomonas sp was used in this study was isolated from a corroding oil tank in an oil depot. Microbial isolates were characterized based on cultural (colonial), microscopic and biochemical methods with reference to standard manuals. (Cheesbrough 2000). The identities of the isolates were cross matched with reference to standard of Bergey’s manual of Determinative Bacteriology (ninth edition). The isolate is a gram-negative, rod-shaped, mobile and non-spore forming aerobic bacteria. The organism isolated physiologically resembles Pseudomonas aeruginosa. It grows optimally at 37 ⁰C. The stock culture was maintained in a medium under nitrogen atmosphere at 4⁰C.

2.1 Plant extract

The extraction of the plant extract was done by Soxhlet extraction method as outlined by [8]. The extracted oil was stored in sterile reagent bottle at 20◦ C prior to use. The amount of plant material extracted was quantified by comparing the weight of the dried residue with the initial weight of the dried plant material before extraction. From the individual stock inhibitor test solutions were prepared in the desired concentration range by diluting with 10% dimethyl sulfoxide (DMSO). The phytochemical screening of the extract was done using standard laboratory procedures as outlined by (Zhang et al 2023).

2.2 Antimicrobial test

The antimicrobial activities of the extracts were tested by agar well diffusion method (Oguzie et al 2012) at 12.5 mg/mL, 25mg/mL, 50 mg/ mL and 100 mg/ mL concentrations. The Petri dishes were filled with cetrimide agar. A loop full of the standardized bacterial culture suspension was evenly spread on the agar surface. Using a sterile cork borer of 6 mm in size, each plate was punched, and 0.1 mL of the extract poured in the bore. Blank hole filled with sterile DMSO was used as control. Each sample was prepared in triplicate. The plates were allowed to stand for 30 minutes and then incubated at 27⁰C for 24hrs. The radius of the zone of inhibition was measured from the edge of the hole to the edge of the zone and recorded as percentage inhibition.

2.3 Corrosion test

The coupons were then suspended with the aid of a rubber thread which passed through the hole in each sample into the cetrimide medium (Control, test organism without extract). The coupons were equally coated with the plant extract and suspended in another medium containing the P. aeruginosa. After a duration of one week, a sample was removed from each medium. The oxide film formed on the surface of the pond was virtually examined, brushed with a sponge in water in order to remove corrosion products and then dried in acetone. The cleaned sample was weighed. The loss of weight in each case was evaluated and tabulated accordingly. This procedure was repeated until the end of the sixth week when the last set of the samples were removed for corrosion inspection and measurement. The rate of corrosion of the samples was monitored and determined by weight loss technique as described by Kumar et al (2012) and Imo et al (2023).

The value of the weight loss and corrosion rate based on weight loss was calculated from the equations (1) and (2) respectively:

∆W= Wo – Wi                                                                             (1)

CR = k ∆WA⍴t                                                                                     (2)

Percentage weight loss     %Wl = Wi -WfWi  x 100                       (3)

A=Exposed surface area =2(LW+LH+HW) cm2, where L= length of the coupon, W= width of the coupon, H= height of the coupon or thickness, k = corrosion rate constant (143,700 mpy), ρ =density of metal coupon (g/cm3), Wo = initial weight, Wi = final weight, ∆W=weight loss of coupon (g); t = time (days).

2.4 Electrochemical tests

The potentiodynamic polarization analysis on copper was carried out at 30 ◦C ambient temperature with a three-electrode system consisting of the mounted copper, Ag/AgCl reference electrode and platinum counter electrode. The electrodes were placed inside a transparent glass cell containing 200 mL of the electrolyte at specific inhibitor concentrations. The electrodes were connected to Gamry 600+ potentiostat linked to computer system. Polarization plots were produced at scan rate of 0.001 V/s between potentials of -2.5 V and +2 V. Corrosion current density, (A/cm2) and corrosion potential, (V) were determined from the plots by Tafel extrapolation method. Corrosion rate (mm/y) was calculated from the equation below:

Corrosion Rate = 0.00327 ˟ CD ˟ EQVD               (4)

EQV is the equivalent weight (g) of working.

Electrochemical Impedance Spectroscopic analysis was performed with a conventional three electrodes cell using Gamry 1010E potentiostat. Platinum electrode was used as the counter electrode, Ag/AgCl in 3 M KCl as the reference electrode, and the copper specimens were used as the working electrode. The area of the exposed area of working electrode in the medium is approximately 1 cm2 (Cu). Prior to each electrochemical study, the frequency range used was from 100mHZ up to 100kHZ and the amplitude was set at 10mV. The experiment was carried out at 4 min open circuit potential (OCP) to attain steady state conditions.

3.0 RESULTS

The phytochemical analysis of ginger (Zingiber officinale) extract revealed a rich composition of bioactive compounds, primarily consisting of terpenes, ketones, and fatty acids according to Table 1. The major components identified include 6-Gingerol (18.529%), 6-Shogaol (15.224%), α-Zingiberene (12.585%), and β-Sesquiphellandrene (10.908%). The high concentrations of 6-Gingerol, Terpenes and 6-Shogaol are particularly noteworthy. These compounds are known for their potent antioxidant, anti-inflammatory, and antimicrobial activities (Adefegha et al 2021, Ekaluno et al 2020).

Table 1. Phytochemical analysis of ginger (Zingiber officinale) extract

| S/N | Components | Concentration (%) |
| --- | --- | --- |
| 1 | 6-Gingerol | 18.529 |
| 2 | 6-Shogaol | 15.224 |
| 3 | α-Zingiberene | 12.585 |
| 4 | β-Sesquiphellandrene | 10.908 |
| 5 | Paradol | 9.639 |
| 6 | β-Bisabolene | 7.274 |
| 7 | ar-Curcumene | 6.758 |
| 8 | α-Farnesene | 5.751 |
| 9 | Hexadecanoic acid | 3.462 |
| 10 | Oleic acid | 4.148 |
| 11 | Linoleic acid | 1.070 |
| 12 | Stearic acid | 1.048 |

Table 2: Antibacterial activity of Zingiber officinale extract against P. aeruginosa.

| Plant extract | Concentration/ Percentage inhibition in mm |  |  |  |
| --- | --- | --- | --- | --- |
| Z. officinale | 100 | 50 | 25 | 12.5 |
|  | 19±1.0 | 12±1.1 | 0 | 0 |

Figures 1 showed the corrosion behaviour of copper in the presence and absence of P. aeruginosa. The gravimetric results showed that the weight loss of copper increased in the presence of the P. aeruginosa when compared with the result in the absence of the bacteria. The corrosion rate also followed the same trend (Figure 2). The highest corrosion rate was observed on the 38 days of exposure.

Figure 1: Weight loss of copper coupons in the presence and absence of P. aeruginosa

Fig. 2: Corrosion rate of copper in the presence and absence of the P. aeruginosa

Figure 3 and 4 shows the weight loss and corrosion rates of copper in the presence and absence of the inhibitor respectively. The plots show that Z. officinale extract effectively retarded copper corrosion at the concentration studied. Furthermore, the corrosion rate observed in the presence of the extract was found to decrease with exposure time.

Figure 3: Weight loss of copper in the presence and absence of Zingiber officinale extract and P. aeruginosa

Figure 4: Corrosion of copper in the presence and absence of Zingiber officinale extract and P. aeruginosa

Table 3 shows the results of the PDP test of copper in the presence and absence of P. aeruginosa. The result showed the corrosion current ( icorr ) increased from 4.620 µA/Cm2 in the absence of the bacteria to 5.730 µA/Cm2in the presence of the bacteria. The corrosion potential (Ecorr) also followed the same trend. The CR of copper also increased from 2.112 mpy in the absence of the P. aeruginosa to 2.620 mpy in the presence of the bacteria.

Figures 5 and 6 show the Tafel plot of the PDP tests of copper in the presence and absence of P aeruginosa.

Table 3: Potentiodynamic Polarization (PDP) for copper in the absence (control) and in the presence of P. aeruginosa

| System | Ecorr (mV) | Icorr (µA/cm2) | CR (mpy) | Beta A e-3V/decade | Beta C e-3V/decade |
| --- | --- | --- | --- | --- | --- |
| Copper in trypticate medium | -796.0 | 4.620 | 2.112 | 432.3 | 395.5 |
| Copper in medium + Pseudomonas aeruginosa | -607.0 | 5.730 | 2.620 | 600.7 | 293.5 |

Key: Ecorr = corrosion potential’; icorr corrosion current; CR = corrosion rate; Beta A = Anodic Tafel slope; Beta C = Catodic Tafel slope; Medium = Tryticate medium; MPY = mil per year.

Figure 5: Tafel plot of the PDP tests of copper in the absence of P. aeruginosa

Figure 6: Figure 5: Tafel plot of the PDP tests of copper in the presence of P. aeruginosa

Table 4 shows the EIS test for copper in the presence of Z. officinale in the medium coated with extract and in the absence of P. aeruginosa.

ELECTROCHEMICAL IMPEDANCE SPECTROSCOPY (EIS) for copper coated with Z. officinale in trypticate medium (control) and in P. aeruginosa

| Parameters | Copper coated with ginger extract in trypticate medium | Copper in medium + P. aeruginosa | Copper coated with ginger extract in P. aeruginosa | Unit |
| --- | --- | --- | --- | --- |
| Rp | 5.19E-04 | 3.15E+04 | 98.69 | Ohms (Ω) |
| Rs | 1.99E-06 | 208.1 | 7.13E-06 | Ohms (Ω) |
| Yo | 4.92E-01 | 2.22E-05 | 4.58E-01 | S*s^a |
| Alpha | 2.08E+04 | 7.06E-01 | 2.02E+04 |  |
| Goodness of fit | 8.45E-03 | 6.27E-03 | 4.08E-03 |  |

Key: Rp = Polarization resistance; Rs = Solution resistance; Yo = Constant phase element

4.0 DISCUSSION

The high concentrations of 6-Gingerol, Terpenes and 6-Shogaol are particularly noteworthy. These compounds are known for their potent antioxidant, anti-inflammatory, and antimicrobial activities (Nazzaro et al 2017 and Anh et al 2020). These findings suggest that the ginger extract has a rich phytochemical profile, with compounds known for their biological activities. This supports its potential use as a biocide and corrosion inhibitor. Table 2 shows the diameters of the zones of inhibition at different concentrations of ginger extract against P. aeruginosa. The undiluted ginger extract showed significant antibacterial activity, with inhibition zones ranging from 18 to 20 mm against P. aeruginosa, suggesting that ginger extract could be a potent natural alternative. At 50% concentration, the extract still exhibited notable antibacterial activity, with inhibition zones between 11 and 13 mm. This indicates that even at half strength, the extract contains sufficient bioactive compounds to inhibit P. aeruginosa growth.

The corrosion behavior of copper in the presence of P. aeruginosa was also investigated. In the P. aeruginosa medium, the weight loss shows a generally decreasing trend over time. The highest weight loss occurs at 14 days (0.057 g), followed by a gradual decrease, with the lowest loss at 35 days (0.045 g). This pattern suggests an initial period of accelerated corrosion, possibly due to the establishment of P. aeruginosa biofilms, followed by a reduction in corrosion rate (Beech & Sunner 2004, Flemming et al 2016). This pattern suggests that corrosion is not a linear process but can be influenced by various factors such as surface conditions, localized environments, and the formation of corrosion products Imo et al 2023. The corrosion rate also shows significant variability. The highest rate is observed at the 28th day, Interestingly, these high corrosion rates do not correspond to the highest weight loss periods. This discrepancy could be due to the formation of protective corrosion products or changes in the surface area exposed to corrosion over time.  The later spikes in corrosion rate could indicate localized breakdown of this protective layer, exposing fresh metal to the medium.

The corrosion rate of copper in the absence of P. aeruginosa shows a more complex pattern. It decreases from 7 to 28 days, then spikes at 35 days (0.004459 mm/yr) before decreasing again at 42 days. This behavior could be related to the dynamics of biofilm formation and the production of corrosive metabolites by P. aeruginosa. However, in the absence of the bacteria, we observed a significant decrease in corrosion with only a slight spike on the 35ft day. Furthermore, the observed peaks in corrosion rate at specific intervals are consistent with the phenomenon of localized corrosion. This suggests that the corrosion process was not uniform across the entire surface of the mild steel samples. Al-Zahrani et al 2016. had previously reported about localized pitting corrosion of mild steel in saline water, highlighting the possibility of non-uniform corrosion even in seemingly homogeneous environments (Eyu et al 2013).

Copper in the presence of the bacteria coated with Z. officinale extract showed significantly lower corrosion rates when compared to the result in the absence of the extract. The findings suggest that natural extracts like Z. officinale could be explored as a more sustainable and environmentally friendly alternative to traditional synthetic corrosion inhibitors (Kasi et al 2024, Kumar et al 2021). The observed fluctuations in weight loss and corrosion rate suggest that the Z. officinale extract's protective effect might be weakened at specific times, potentially due to biofilm formation, extract degradation, and environmental factors (Obike et al 2017, Okafor et al 2007, Okon et al 2021, El-Etre, 2003)

The potentiodynamic polarization results of P. aeruginosa influenced corrosion of copper showed that the icorr increased in the presence of the bacteria (4.620 μA) compared to (5.730 μA) observed in the absence of the bacteria. The anodic value (600.7e-3 V/decade) in presence of the bacteria was also higher than the cathodic value (432.3e-3 V/decade) in absence of the bacteria. This result corresponds with previous gravimetric results. Videla, 2021 reported that any biological effect that facilitates the anodic reaction or that separates the anodic and cathodic sites, will increase corrosion. It is possible that the presence of P. aeruginosa on the copper could have increased the anodic reaction leading to increase in anodic current and subsequently to the corrosion of the metal. Mansfield et al. (2002) used potentiodynamic polarization technique to examine the overall corrosion behavior of a corrosion system. The authors observed that increase in Icorr was due to the influence of microorganisms on the rate of the anodic and cathodic reactions Imo and Nwokorie 2021; Oguzie et al 2023)

The potentiodynamic polarization curve (Fig. 5 and 6) of copper in the presence and absence of P. aeruginosa showed no distinct difference on the cathodic branch but the anodic branch changed quite slightly suggesting that the anodic site was more sensitive to corrosion with the resultant metal dissolution.

The EIS of copper in the presence of P. aeruginosa without the extract and copper coated with extract in the presence of the bacteria showed clear variations in Rp (3.15 × 10⁴ Ω and 98.69 Ω) respectively. Because Rp is a measure of a material’s resistance to electrochemical reaction, the results obtained showed that the Rp increased with the coating of the mild steel with the extract. Beech (2004) reported that the presence of inhibitor increases the Rp of a metal. This might be the reason for the increase in Rp observed in the presence of the extract. Studies show that the protective layer formed by the inhibitor impedes the flow of current associated with corrosion thereby increasing the resistance to electrochemical reaction.

5.0 CONCLUSION

This study establishes Zingiber officinale extract as an effective green biocide for mitigating Pseudomonas-induced corrosion of copper in microbiologically active environments. The observed inhibition is attributed to the combined effects of microbial suppression and the formation of a protective adsorbed layer on the copper surface. These findings position ginger extract as a viable, environmentally sustainable alternative to conventional biocides for MIC control in copper-based systems.

DECLARATION OF COMPETING INTEREST

The authors declare that they have no known competing financial interests or personal relationships that would influence this paper.

Disclaimer (Artificial intelligence)

Author(s) hereby declare that no generative AI technologies have been used during the writing or editing of this manuscript.

REFERENCES

Anh, N.H., Kim, S.J., Long, N.P., Min, J.E., Yoon, Y.C., Lee, E.G., Kim, M., Kim, T.J., Yang, Y.Y., Son, E.Y. & Yoon, S.J. (2020). Ginger on human health: A comprehensive systematic review of 109 randomized controlled trials. Nutrients, 12(1), 157. https://doi.org/10.3390/nu12010157

Al-Zahrani, A.M., Al-Amri, M.A. & El-Shehabi, M.M. (2016). Corrosion behaviour of mild steel in saline water. Journal of Materials Science and Engineering B, 3(4), 189-196.

Avelino-Jiménez, I.A., Hernández-Maya, L., Larios-Serrato, V., Quej-Ake, L., Castelán-Sanchez, H., Herrera-Dìaz, J., Garibay-Febles, V., Rivera-Olvera, J.N., Zavala-Olivares, G., Zapata-Peñasco, I. (2023). Biofouling and biocorrosion by microbiota from a marine oil pipeline: A metagenomic and proteomic approach. Journal of Environmental Chemical Engineering, 11(2), 109413.

Cheesbrough, M. (2000). Microbial Tests in: Cheesbrough, M. Ed., District Laboratory Practice in Tropical Countries, Part 11, Low Priced Edition, Cambridge University Press, Cambridge, 105-130.

Cheesbrough, M. (2000). Microbiological Tests in: Cheesbrough, M. Ed., District Laboratory Practices in Tropical Countries, Part 11, Low Priced Edition, Cambridge University Press, Cambridge, 105-130.

Beech, I.B. (2004). Corrosion of technical materials in the presence of biofilms- current understanding and state-of-the –act methods of study. International Journal of Bioderioration and Biodegredation 53: 177-183

Beech, I.B. & Sunner, J. (2004). Biocorrosion: towards understanding interactions between biofilms and metals. Current Opinion in Biotechnology, 15(3), 181-186. https://doi.org/10.1016/j.copbio.2004.05.001.

Dang, H. & Lovell, C.R. (2016). Microbial Surface Colonization and Biofilm Development in Marine Environments. Microbiology and Molecular Biology Reviews, 80, 91-138. https://doi.org/10.1128/MMBR.00037-15.

El-Etre, A.Y. (2003). Inhibition of aluminum corrosion using Opuntia extract. Corrosion Science, 45(11), 2485-2495. https://doi.org/10.1016/S0010-938X(03)00066-0

Eyu, D.G., Hamazah, E., Ismail, M., Abdulrahman, A.S., & Mohammad A. (2013). Effect of Vernonia Amygdalina extract on corrosion inhibition of mild steel in simulated seawater. Australian Journal of Basic and Applied Sciences, 7(14), 257-263.

Flemming, H.C., Wingender, J., Szewzyk, U., Steinberg, P., Rice, S.A. & Kjelleberg, S., (2016). Biofilms: an emergent form of bacterial life. Nature Reviews Microbiology, 14(9), 563-575. https://doi.org/10.1038/nrmicro.2016.94

Fontana M.G. (2005). Corrosion Engineering fourth ed., Tata Mc Graw-Hill Book company New York.

Imo E.O. and Nokorie, R.C. (2021). A review of fungal corrosion of metals. Zastita Materijala 62 (4), 333-339.

Imo, E.O., Ihejirika, C.E., Ndukaku, A.G. Misoni, P.J. (2023).  Effects of Desulfotomaculum sp on corrosion behaviour of mild steel and aluminium in sea water. Zastita Materijala 64 (2) 190 – 197.

Kasi, R.V., Ikenga, B., Nmesoma, A., Bliss, A., Excel M.T., & Collins, E.C. (2024). Antimicrobial properties of ginger (Zingiber officinale L.) and garlic (Allium sativum) on Staphylococcus aureus and Pseudomonas aeruginosa. European Journal of Microbiology and Infectious Diseases, 1(4), 153-164. 10.5455/EJMID.20241011105548

Kumar, A., Tiwari, A.K., Sharma, A. & Singh, P. (2021). Antibacterial activity of ginger (Zingiber officinale) rhizome extract against some gram-negative and gram-positive bacteria. Journal of Pharmacognosy and Phytochemistry, 10(3), 31-34.

Kumar, R.K.S., Vijian, P., Solomon, J.S., & Benchmans, I.J. (2012). Corrosion studies on stainless steel. International Journal of Emerging Technology and Advanced Engineering 2(5): 178-182.

Mansfield, A.P., Shib, Devinny, H.J., Islander, R. and Chan, C.L. (2002). Corrosion monitoring and control for concrete sewer pipes. Corrosion, 90.

Marzorati, S., Verotta, L., & Trasalti, S.P. (2019). Green Corrosion Inhibitors from Natural Sources and Biomass Wastes. Molecules, 24(1): 48.

Nazzaro, F., Fratianni, F., Coppola, R. & De Feo, V. (2017). Essential oils and antifungal activity. Pharmaceuticals, 10(4), 86. https://doi.org/10.3390/ph10040086.

Nwokorie, R.C., Ogbulie, J.N., Nweke, C.O, Akujobi, C.O., Imo, E.O. (2025). Microbial influenced corrosion of copper and inhibiting effects of Capsicum annuum extracts. Intl. of Innovative Sci. and Resch. Tech. 10 (3) 3269-3274.

Oguzie E.E., Oguzie K.L., Akalezi C.O., Udeze I.O., Ogbulie J.N., & Njoku V.O. (2012). Natural Products for Materials Protection: Corrosion and Microbial Growth Inhibition Using Capsicum Frutescens Biomass Extracts. ACS Sustainable Chemistry and Engineering, 1(2), 214-225. DOI:10.1021/sc300145k

Obike, A.I., Okorie, N.A., Edeke, S.O., & Ezealor, A.U. (2017). Alligator Pepper (Aframomum melegueta) Extracts as Corrosion Inhibitors for Mild Steel in Simulated Oilfield Environment Containing Desulfovibrio desulfuricans. Journal of Bio- and Tribo-Corrosion, 3(4), 53.

Okafor, P. C., Osabor, V. I., & Ebenso, E. E. (2007). Eco-friendly corrosion inhibitors: Inhibitive action of ethanol extracts of Garcinia kola for the corrosion of mild steel in H2SO4 solutions. Pigment & Resin Technology, 36(5), 299-305.

Okon, A.N., Udoh, I.I, & Eduok. U.M. (2021). Mechanistic study of corrosion inhibition of mild steel by Aframomum melegueta extracts in the presence of Desulfovibrio desulfuricans. Journal of Bio- and Tribo-Corrosion, 7(1) Chemistry

Oparaodu, K.O. & Okpakwasili, G.C. (2014). Comparison of percentage weight loss and corrosion rate trends in different metal coupons from two soil environments. International Journal of Environmental Bioremediation and Biodegradation, 2(5), 243-249. Doi:10.12691/ijebb-2-5-5.

Prasad, S. & Tyagi, A.K. (2015). Ginger and its constituents: role in prevention and treatment of gastrointestinal cancer. Gastroenterology Research and Practice, 2015(1), 142979. https://doi.org/10.1155/2015/142979.

Shi, X., Zhang, R., Sand, W., Mathivanan, K., Zhang, Y., Wang, N., Duan, J., & Hou, B. (2023). Comprehensive Review on the use of Biocides in Microbiologically influenced corrosion. Microorganisms, 11(9), 2194. doi:10.3390/microorganisms11092194.

Videla, H.A. & Herrera, L.K. (2005). Microbiologically influenced corrosion: looking to the future. International Microbiology, 8(3), 169. https://doi.org/10.2436/im.v8i3.9508.

Videla, H.A. (2001). Microbially influenced corrosion: an update overview. Int. Biodeterior Biodegradation. 48: 176-201.

Wen, Y., Liu, Q., Wang, J., Yang, Q., Zhao, W., Qiao, B., Li, Y., & Jiang, D. (2021). Improving vitro and in vivo corrosion resistance and biocompatibility of Mg-1Zn-1Sn alloys by microalloying with Sr. Bioactive Materials, 6(12), 4654-4669. http://doi.org/10.1016/j.bioactmat.2021.04.043

Zhang, M. Zhao, J., Dai, X. Li, X. (2023). Extraction and Analysis of Chemical Compositions of Natural Products and Plants. Separations 2023, 10, 598. https://doi.org/10.3390/ separations10120598.

Wang, Y., Zhao, Y., Xue, F., Nan, X., Wang, H., Hua, D., Liu, J., Yang, L., Jiang, L. & Xiong, B. (2020). Nutritional value, bioactivity, and application potential of Jerusalem artichoke (Helianthus tuberosus L.) as a neoteric food: A review. Food Chemistry, 339, 128023. https://doi.org/10.1016/j.foodchem.2020.128023