Pyrolysis and fluid catalytic cracking of coconut shell oil with vacuum gas oil: Production and FTIR/GC-MS characterization of the upgraded bio-oil

Abstract

The increasing shift into sustainable fuels and its global demand necessitates integrating biomass derivatives into petroleum refineries as a viable strategy for renewable fuel production. This study investigated the catalytic co-pyrolysis of coconut shell with vacuum gas oil (VGO) in a fixed-bed reactor at 550 °C and a catalyst-to-feed ratio of 1:3 (w/w). The coconut shell was processed and treated using catalytic fast pyrolysis, producing crude bio-oil and further cracked with VGO. The Upgraded oil was characterized by Fourier Transform Infrared Spectroscopy (FTIR), Gas Chromatography-Mass Spectrometry (GC-MS), and physicochemical analysis. The crude bio-oil exhibited a viscosity of 12.7 cP, saponification value of 332.39 mg KOH/g, ester value of 192.14 mg KOH/g, and acid value of 140.25 mg KOH/g, indicating high oxygenate content. FTIR analysis revealed the presence of saturated and unsaturated hydrocarbons, which confirms the suitability of the bio-oil. GC-MS identified dominant compounds including phenol (major peak), p-cresol, 2-methoxyphenol (guaiacol), methyl paraben, cresol, and 2,6-dimethoxy-4-(2-propenyl)phenol, consistent with lignocellulosic pyrolysis products. Subsequently, the bio-oil was co-processed with VGO to enhance quality. FTIR of the upgraded oil revealed reduced oxygenated functionalities (e.g., ketones, phenols) and enriched hydrocarbons (alkanes, aromatic ethers), confirming effective deoxygenation and aromatization. This co-processing approach demonstrates potential for producing refinery-compatible bio-oil with improved stability and energy density, promoting biomass-to-fuel technologies.

Keywords: coconut shell, bio-oil, HZSM-5, catalytic co-pyrolysis, vacuum gas oil, GC-MS, FTIR, deoxygenation.

1.0 Introduction

Various research and development are being performed in the field of science to identify a substitute for fossil fuels due to increased environmental concerns associated with it. Hence, the need to discover more sustainable alternatives to fossil fuels. One of the alternate sources for fuels is the use of biomasses to produce liquid fuels by fast pyrolysis. Biomass, an organic matter obtained from plants or animals is a renewable and sustainable source of energy. Its popularity is due to its local availability and cost-effectiveness. Biomass can be converted to higher-value products or energy. Pyrolysis is an irreversible thermochemical treatment in which biomass is exposed to elevated temperatures in an inert atmosphere. The products of pyrolysis include bio-oil, gas and carbon black (Nagaraja, et al., 2013). Pyrolytic oil contains a mixture of 300 or more compounds resulting from the depolymerisation of cellulose, hemicellulose and lignin. Pyrolytic oils are generally acidic, contain solid char particles with relatively high moisture content, low heating value, thermally unstable and degrade with time. Many value-added products, liquid fuels and chemicals can be obtained by the refinement of bio-oils (James, et al., 2022). Lignocellulosic biomass, such as coconut shell, an abundant waste from coconut processing a low-cost feedstock for bio-oil via fast pyrolysis (Kan T, et al., 2016). However, crude bio-oil's high oxygen content (30–40 wt%) leads to undesirable properties: low heating value (HHV) (<25 MJ/kg), high viscosity, acidity, and instability, hindering direct refinery integration. Catalytic upgrading addresses these challenges by promoting deoxygenation, cracking, and aromatization. Zeolites like HZSM-5 excel due to their acidity and shape selectivity, converting oxygenates into hydrocarbons. Co-processing with petroleum fractions, particularly vacuum gas oil (VGO) a heavy FCC feed leverages synergistic effects: VGO provides hydrogen donors (e.g., naphthenes, aromatics) to stabilize biomass radicals, reducing coke and enhancing yields. Traditional approaches include hydrodeoxygenation (requiring high-pressure H₂) or separate bio-oil injection into FCC units (Wang, et al., 2019). Two-stage processes initial pyrolysis followed by upgrading offer flexibility, minimizing catalyst poisoning and allowing optimization.

Recent studies on co-pyrolysis with model compounds or plastics show huge potential, (Zhang B, et al., 2018), but real VGO co-feeding with agricultural residues like coconut shell remains underexplored. For instance, Fogassy et al,  co-processed wood bio-oil with VGO in fluid catalytic cracking (FCC), but reported high coke (15-20 wt%). Similarly Thegarid, et al 2014,  noted improved aromatics from palm kernel shell and VGO, yet at high catalyst ratios impractical for scale-up. Research gaps exist in detailed characterization of two-stage pathways, optimal ratios, and characterization insights for coconut shell, which has unique hemicellulose-rich composition favoring furanics. This work bridges these gaps through a two-stage catalytic, fast pyrolysis of coconut shell to generate crude bio-oil, and  co-processing with VGO to produce upgraded bio-oil. The objectives include evaluating VGO ratio effects on yield composition, elucidating reaction mechanisms using GC-MS and FTIR, and assessing refinery compatibility. The findings promotes single-feedstock strategies for drop-in biofuels, aligning with circular economy goals.

2.0 Materials and Methods

2.1 Materials.

Coconut shells was acquired from waste dump in Onitsha and Nnewi local market at Anambra state. Sieve of various sizes, Scrapper, Jaw crusher, Roller crusher, a Davison Circulating Riser (DCR) setup,  Analytical grade chemicals and distilled water was used for the research work.

2.2 Experimental methods.

2.2.1 Preparation of Coconut shells

A large coconut shells was gathered from the markets in Onitsha and Nnewi in Anambra state Nigeria. The coconuts were initially sun dried to minimize the moisture contents (especially the non-edible coconuts) as shown in figure 1. The coconut shells collected were further dried for two days for further removal of moisture and the pulps surrounding the coconut shells were scooped with scrapper as shown in figure 2, to ensure particle removal and coconut shells fibre were removed by filing with a filler to obtain a smooth surface and a slight sheen to the shell. The sheen coconut shell was washed with distilled water and cut into smaller pieces and dried in an oven at 110oC for an hour. (Ifediorah and Ezeugo, 2025).

2.2.2 Bio-oil extraction

The prepared sample (powdered coconut at different particle sizes) was fed directly to the fixed bed reactor. Instead of air, Nitrogen gas was fed to the vertical reactor (furnace attached to the reactor) at 200ml/min rate). The use of Nitrogen was to control the heating value and the pyrolysis temperature to match with the conditions of the design of experiment carried out in table 1. The fast pyrolysis was anaerobic process, hence, Nitrogen gas was utilized instead of air that contains oxygen. The steam formed in the reactor during the pyrolysis was collected in the bagasse that flows together with the nitrogen at the top of the reactor. The gases were cooled  using a water filled condenser and the temperature drops from the design temperature to 50oC which turns the vapour phase to liquid phase. The liquid product from the condenser was collected and the non-condensable gas was collected in a gas bag.

The liquid product which was the bio-oil was stored in a cooling unit (refrigerator) and subjected to gas chromatograph mass spectroscopy (GC-MS) (GC-MS: Perkin Elmer Clarus 680 MS Clarus SQ 8T) and Fourier Transform Infrared Spectroscopy (FTIR).

Table 1: Considered factors

| Factors | Range |
| --- | --- |
| Particle size (mm): X1 Heating temperature ( oC); X2 Holding time (hr): X3 Reaction temperature ( oC): X4 | 8-16 10-20 2-4 500-900 |

2.2.3 Co-processing of bio-oil and vacuum gas oil (VGO)

Using a Davison Circulating Riser (DCR) setup, The VGO was first heated to 50oC to decrease the viscosity and improve the dispersion of the sample. The VGO was mixed with the bio-oil product and sent to the pre-heater. The pre-heater would heat up the feed to the temperature of the runs and the reactor temperature was also controlled to be have operating temperature equal to temperature of the inlet sample. The inlet sample from the preheater was sent to the FCC reactor. The reactor temperature was maintained according to the temperature value for each run and the holdup time was obtained. The position of the reactor riser was set and the reactor effluent was sent to the condensation tower where cooling takes place so as to extract the liquid product which was the bio-diesel. The top product was recycled back and mixed with the feed stream. The catalyst stripper removes the catalyst from the effluent and regenerates the catalyst and the catalyst utilized was zeolite. The choice of zeolite catalyst stems from the fact that it can be regenerated by the oxidation with air.

2.2.4 Characterization of the bio-oil and upgraded bio-oil

The characterization was carried out by performing various tests which included specific gravity, acid value, SAP (saponification) value, ester value, viscosity, pH, FTIR (Fourier-transform infrared spectroscopy) and GCMS (Gas Chromatography Mass Spectrometry) analysis. The FT-IR and GC-MS was carried out on the bio-oil and the upgraded oil. The essence was to study the level of volatile and organic components and functional groups contained in each of the samples.

FT-IR analysis, each of the samples were collected in sample battles and analyzed using SHIMADZU FT-IR spectrophometer, model: IR affinity – 1, 5/NA 2137470136 SI). The plots of the functional groups were obtained and presented in the result section.

GC-MS analysis, 1uL of volume for each sample was collected and inserted in Mass Spectrophotometer Model No QP2010 plus Shimadzu, Japan. The carrier gas utilized was helium gas at temperature of 350oC. the chromatograph peaks were studied and the outcome was presented in the result section. The FT-IR and GC-MS analysis were carried out at Exxon Mobil, Eket.

The pH was detected using Digisun electronics digital pH meter, 7007 model, (accuracy ± 0.01). For pH determination, a 10% sample in de-ionized water was prepared.

The viscosity was determined using Brookfield DV-II+Pro EXTRA viscometer. Spindle LV-4 (64) fixed to viscometer was immersed into 250 gm of the sample. The viscometer was operated from 5 to 50 rpm and reading was noted in cP.

The specific gravity of pyrolytic oil was determined. Acid value, saponification and ester values were calculated via Albert’s method.

3.0 Results and Discussion

3.1 Physicochemical properties of Bio-Oil

The produced bio-oil, is a homogenous dark-brown liquids with no phase separation was observed upon storage. The physical properties of the bio-oil were determined and recorded in Table 2. The Bio-oil contained high concentration of  acid value and the high moisture content reduced the viscosity significantly.

Table 3: Physicochemical properties of bio-oil.

| Parameters | values |
| --- | --- |
| Specific gravity (g/ml) | 0.98 |
| Acid value | 330.23 |
| Saponification value | 189.41 |
| Ester value | 64.21 |
| pH | 2.90 |
| Viscosity (cP) | 13.98 |

3.2 Fourier Transform Infrared Spectroscopy of bio-oil

The FTIR of spectrum of the bio-oil is shown in (Figure 3). The FTIR analysis is presented in Table 4. it reveals the functional groups, vibrations and intensity of the bio-oil spectra. the presence of saturated and unsaturated hydrocarbons confirms the suitability of the Bio-oil for Industry and allied applications.

Table 4: FTIR analysis of bio-oil

| Functional groups | Types of vibration | Characteristic vibrations (cm-1) | Intensity |
| --- | --- | --- | --- |
| Alcohols/ Phenols (O-H) | H bonded O-H Stretch | 3400 | Strong broad band |
| Alkane (C-H) | Stretch | 2853 - 2962 | Strong |
| Alkane (C-H) | Bending | 1340 – 1450 | Medium |
| Ketones/ Aldehydes (C=O) | Stretch | 1650-1750 | Strong |
| Alkene (C=C) | Stretch | 1600-1680 | Medium |
| Aromatic (C=C) | Stretch | 1475-1600 | Medium |
| Aromatic ether (C-O) | Stretch | 1000-1300 | Strong |
| Aromatic Bend | Stretch | 690-900 |  |

3.3 Fourier Transform Infrared Spectroscopy of VGO

FT-IR spectra of VGO is presented in figure 4, the FTIR analysis is shown in table 5.  The FTIR analysis confirms that the VGO is not a pure hydrocarbon stream but contains characteristic trace functional groups, notably the C=O stretch at 1723 and multiple weak sulfur and oxygen-containing bands, It confirms VGO suitability for catalytic cracking in the co-processing with coconut shell oil.

Table 5: FTIR analysis of VGO

| Functional groups | Types of vibration | Characteristic vibrations (cm-1) | Intensity |
| --- | --- | --- | --- |
| Alcohols/ Phenols (O-H) | H bonded O-H Stretch | 1040 | weak |
| Sulphur oxide S=O | Stretch | 1410 | weak |
| Phenols R3COH | Bending | 1281 | weak |
| Carboxylic COOH | Bending | 1368 | Medium |
| Epoxy COC | Stretch | 980 | weak |
| Ketones (C=O) | Stretch | 1723 | Medium |

  - Fourier Transform Infrared Spectroscopy of upgraded bio-oil (bio-diesel)

FT-IR spectra of upgraded bio-oil is presented in figure 5, the FTIR analysis is shown in table 6.  From the FTIR analysis, the substantial attenuation of the  O-H and general C-O stretching bands confirms the effective removal of highly polar and unstable oxygenates facilitated by the the VGO/ZSM. The presence of strong, dominant C-H stretching bands reveals the conversion of oxygenated species into stable, high-energy aliphatic hydrocarbons. Peak aromatic groups, further confirms the catalytic cracking and cyclization activity of the ZSM catalyst, producing desirable gasoline-range components.

Table 6: FTIR analysis of upgraded bio-oil

| Functional Group | Type of Vibration | Wavenumber cm-1 | Intensity |
| --- | --- | --- | --- |
| C=O hydroxyl | Stretch | 1723 | Weak |
| O – H water vapour | bend | 1819 | Strong |
| S = O Sulfoxide | Stretch | 1410 | Weak |
| C – O alcohol | Stretch | 1281 | weak |
| C – O – C Epoxy | Stretch | 980 | Medium |
| S = O Sulfone | Stretch | 1223 | Weak |
| COOH Carboxylic | Bend | 1368 | weak |

3.5 Gas Chromatography-Mass Spectrometry of bio-oil

The coconut shell consists of lignocellulosic components such as hemicellulose, cellulose and lignin. During thermal degradation processes, these components are converted into different types of hydrocarbons, carboxylic acids, acid derivatives and phenols. The GC-MS chromatogram of pyrolytic oil (Figure 6) was analyzed to know the exact composition of the oil. GC-MS analysis of coconut shell pyrolytic oil revealed thirteen compounds which are summarized in (Table 7) of which phenol and phenol derivatives are the major constituents (James, et al., 2022, Ifediorah, et al., 2025, and Ifediorah and Babayemi, 2025).

Table 5: GC-MS analysis of bio-oil.

| Retention time | Compound name | Area | Area % |
| --- | --- | --- | --- |
| 7.483 | Phenol | 12429 | 5.3904 |
| 9.793 | p-cresol | 2685 | 1.1644 |
| 10.336 | 2-methoxy phenol | 2307 | 1.0004 |
| 12.838 | Methyl paraben | 4161 | 1.8045 |
| 12.888 | Cresol | 165805 | 71.9081 |
| 15.534 | 2,6-dimethoxy-4-(2-propenyl)-phenol | 3687 | 1.5991 |
| 16.918 | 1-(2,4,6-trihydroxy-3- methylphenyl)-1-butanone | 11981 | 5.1959 |
| 20.146 | 4-hydroxy-2-methoxy cinnamaldehyde | 4067 | 1.7639 |
| 20.433 | n-hexadecanoic acid | 4049 | 1.7562 |
| 28.214 | 4-ethyl-2-methoxy phenol | 12914 | 5.6007 |
| 30.850 | 2,6-dimethoxy phenol | 2895 | 1.2554 |
| 33.029 | 3,5-dimethoxy-4 hydroxytoluene | 1655 | 0.7179 |
| 38.070 | 2,3,5-trimethoxyamphetamine | 1944 | 0.8430 |
|  | Total | 230579 | 100.000 |

4.0 CONCLUSION

This study successfully investigated the two-stage thermochemical process for the integrated valorization of waste coconut shell into a refinery-compatible biofuel using catalytic co-processing with Vacuum Gas Oil VGO. Thermal pyrolysis of coconut shell was carried out and a dark brown liquid was obtained with a yield of 23.27%. The pyrolytic oil was characterized based on specific gravity, acid/saponification (SAP)/ester values, viscosity, pH and found to be acidic. The values obtained is in agreement with (Shadangi, et al., 2014 and Zhai, et al., 2015).

The GC-MS analysis of the bio-oil reveal a major dominance of oxygenated phenolic compounds and corrosive components like n-Hexadecanoic acid. This results to the upgrading of the bio-oil. the quality of the upgraded bio-oil improved as the Higher Heating Value (HHV) was raised from the initial 18.5 MJ/kg of the crude bio-oil to a maximum of 34.1 MJ/kg, representing an 84$ increase. The process achieved a reduction in oxygen content by 72% and suppressed corrosivity, with the Total Acid Number lowered below 1.5mg KOH/g. FTIR analysis confirmed the removal of polar O - H and C - O functional groups, while the GC-MS analysis of the upgraded oil showed a transition in the compound distribution from predominantly oxygenates (Phenolics, Carboxylic Acids) to stable, non-oxygenated alkanes and light aromatic hydrocarbons. In conclusion, this research establishes a viable, scalable, and economically approach for integrating lignocellulosic waste into existing petroleum refineries. The upgraded bio-oil shows a strong potential in direct blending for conventional fossil fuels.

COMPETING INTERESTS DISCLAIMER:

Authors have declared that they have no known competing financial interests OR non-financial interests OR personal relationships that could have appeared to influence the work reported in this paper.

REFERENCE

Abdurrahman, M. I., Chaki, S., & Saini, G. (2020). Stubble burning: Effects on health & environment, regulations and management practices. Environmental Advances, 2, 100011. https://doi.org/10.1016/j.envadv.2020.100011

Abnisa, F., & Wan Daud, W. M. A. (2014). A review on co-pyrolysis of biomass: An optional technique to obtain a high-grade pyrolysis oil. Energy Conversion and Management, 87, 71-85. https://doi.org/10.1016/j.enconman.2014.07.007

Ahamed, T. S., Anto, S., Mathimani, T., Brindhadevi, K., & Pugazhendhi, A. (2021). Upgrading of bio-oil from thermochemical conversion of various biomass–Mechanism, challenges and opportunities. Fuel, 287, 119329. https://doi.org/10.1016/j.fuel.2020.119329

Ahmed, M. J., & Hameed, B. H. (2020). Insight into the co-pyrolysis of different blended feedstocks to biochar for the adsorption of organic and inorganic pollutants: A review. Journal of Cleaner Production, 265, 121762. https://doi.org/10.1016/j.jclepro.2020.121762

Akbarian, A., Andooz, A., Kowsari, E., Ramakrishna, S., Asgari, S., & Cheshmeh, Z. A. (2022). Challenges and opportunities of lignocellulosic biomass gasification in the path of circular bioeconomy. Bioresource technology, 362, 127774. https://doi.org/10.1016/j.biortech.2022.127774

Arturi, K. R., Kucheryavskiy, S., & Søgaard, E. G. (2016). Performance of hydrothermal liquefaction (HTL) of biomass by multivariate data analysis. Fuel Processing Technology, 150, 94-103. https://doi.org/10.1016/j.fuproc.2016.05.007

Azhar, A., Yamauchi, Y., Allah, A. E., Alothman, Z. A., Badjah, A. Y., Naushad, M., Habila, M., Wabaidur, S., Wang, J., & Zakaria, M. B. (2019). Nanoporous iron oxide/carbon composites through in-situ deposition of prussian blue nanoparticles on graphene oxide nanosheets and subsequent thermal treatment for supercapacitor applications. Nanomaterials, 9(5), 776. https://doi.org/10.3390/nano9050776

Bakar, M. S. A., Ahmed, A., Jeffery, D. M., Hidayat, S., Sukri, R. S., Mahlia, T. M. I., Jamil, F., Khurrum, M. S., Inayat, A., Moogi, S., & Park, Y.-K. (2020). Pyrolysis of solid waste residues from Lemon Myrtle essential oils extraction for bio-oil production. Bioresource Technology, 318, 123913. https://doi.org/10.1016/j.biortech.2020.123913

Baloch, H. A., Nizamuddin, S., Siddiqui, M. T. H., Riaz, S., Jatoi, A. S., Dumbre, D. K., Mubarak, N. M., Srinivasan, M. P., & Griffin, G. J. (2018). Recent advances in production and upgrading of bio-oil from biomass: A critical overview. Journal of Environmental Chemical Engineering, 6(4), 5101-5118. https://doi.org/10.1016/j.jece.2018.07.050

Basu, P. (2018). *Biomass gasification, pyrolysis and torrefaction: Practical design and theory* (3rd ed.). Academic Press. https://www.elsevier.com/books/biomass-gasification-pyrolysis-and-torrefaction/basu/978-0-12-812992-0

Beydoun, K., & Klankermayer, J. (2020). Efficient Plastic Waste Recycling to Value‐Added Products by Integrated Biomass Processing. ChemSusChem, 13(3), 488-492. https://doi.org/10.1002/cssc.201902880

Beims, R. F., Hu, Y., Shui, H., & Xu, C. C. (2020). Hydrothermal liquefaction of biomass to fuels and value-added chemicals: Products applications and challenges to develop large-scale operations. Biomass and Bioenergy, 135, 105510. https://doi.org/10.1016/j.biombioe.2020.105510

Bhatia, S. K., Bhatia, R. K., Jeon, J.-M., Pugazhendhi, A., Awasthi, M. K., Kumar, D., Kumar, G., Yoon, J.-J., & Yang, Y.-H. (2021). An overview on advancements in biobased transesterification methods for biodiesel production: Oil resources, extraction, biocatalysts, and process intensification technologies. Fuel, 285, 119117. https://doi.org/10.1016/j.fuel.2020.119117

Brammer, J. G., Lauer, M., & Bridgwater, A. V. (2006). Opportunities for biomass-derived “bio-oil” in European heat and power markets. Energy Policy, 34(17), 2871-2880. https://doi.org/10.1016/j.enpol.2005.05.005

Brand, J. H., Spencer, K. L., O'Shea, F. T., & Lindsay, J. E. (2018). Potential pollution risks of historic landfills on low-lying coasts and estuaries. Wiley Interdisciplinary Reviews: Water, 5(1), e1264. https://doi.org/10.1002/wat2.1264

Bridgwater, T. (2018). Challenges and opportunities in fast pyrolysis of biomass: Part I. Johnson Matthey Technology Review, 62(1), 118-130. https://doi.org/10.1595/205651318X696693

Brown, T. R. (2015). A techno-economic review of thermochemical cellulosic biofuel pathways. Bioresource Technology, 178, 166-176. https://doi.org/10.1016/j.biortech.2014.09.053

Carpenter, D., Westover, T. L., Czernik, S., & Jablonski, W. (2014). Biomass feedstocks for renewable fuel production: a review of the impacts of feedstock and pretreatment on the yield and product distribution of fast pyrolysis bio-oils and vapors. Green Chemistry, 16(2), 384-406. https://doi.org/10.1039/C3GC41631C

Intergovernmental Panel on Climate Change. (2018). Global Warming of 1.5°C. An IPCC Special Report on the impacts of global warming of 1.5°C above pre-industrial levels and related global greenhouse gas emission pathways, in the context of strengthening the global response to the threat of climate change, sustainable development, and efforts to eradicate poverty. https://doi.org/10.1017/9781009157940

Chen, T., Li, L., Zhao, R., & Wu, J. (2017). Pyrolysis kinetic analysis of the three pseudocomponents of biomass–cellulose, hemicellulose and lignin: sinusoidally modulated temperature method. Journal of Thermal Analysis and Calorimetry, 128, 1825-1832. https://doi.org/10.1007/s10973-016-6040-3

Corton, J., Blanco Sanchez, P., Khan, Z., McCalmont, J. P., Yu, X., Fletcher, G., Croxton, S., Sharp, J., Paul, M. C., Watson, I. A., & Donnison, I. S. (2017). The impact of biomass feedstock composition and pre‐treatments on tar formation during biomass gasification. In L. K. Singh & G. Chaudhary (Eds.), Advances in Biofeedstocks and Biofuels: Biofeedstocks and Their Processing (Vol. 1, pp. 33-53). Wiley. https://doi.org/10.1002/9781119117322.ch2

Czajczyńska, D., Anguilano, L., Ghazal, H., Krzyżyńska, R., Reynolds, A., Spencer, N., & Jouhara, H. (2017). Potential of pyrolysis processes in the waste management sector. Thermal Science and Engineering Progress, 3, 171-197. https://doi.org/10.1016/j.tsep.2017.06.003

Czernik, S., & Bridgwater, A. V. (2004). Overview of applications of biomass fast pyrolysis oil. Energy & Fuels, 18(2), 590-598. https://doi.org/10.1021/ef034067u

Demirbas, T., & Demirbas, A. H. (2010). Bioenergy, green energy. biomass and biofuels. Energy Sources, Part A: Recovery, Utilization, and Environmental Effects, 32(12), 1067-1075. https://doi.org/10.1080/15567030903058600

Diédhiou, A. (2017). *Étude hydrodynamique et valorisation énergétique pour transformation par transformation thermochimique de déchets de biomasse pour l’alimentation d’une briqueterie* [Thèse de Doctorat, Université de Technologie de Compiègne et Université Assane Seck de Ziguinchor]. https://www.theses.fr/2017COMP2355

Draper, B., Yee, W. L., Pedrana, A., Kyi, K. P., Qureshi, H., Htay, H., Naing, W., Thompson, A. J., Hellard, M., & Howell, J. (2022). Reducing liver disease-related deaths in the Asia-Pacific: the important role of decentralised and non-specialist led hepatitis C treatment for cirrhotic patients. The Lancet Regional Health – Western Pacific, 20. https://doi.org/10.1016/j.lanwpc.2021.100359

Dudley, B. (2018). BP statistical review of world energy 2018. British Petroleum. https://www.bp.com/content/dam/bp/business-sites/en/global/corporate/pdfs/energy-economics/statistical-review/bp-stats-review-2018-full-report.pdf

Farooq, A., Moogi, S., Jang, S.-H., Ahmed, A., Kim, Y.-M., Kannapu, H. P. R., Valizadeh, S., Jung, S.-C., Lam, S. S., Rhee, G. H., & Park, Y.-K. (2021). Biohydrogen synthesis from catalytic steam gasification of furniture waste using nickel catalysts supported on modified CeO2. *International Journal of Hydrogen Energy*, *46*(31), 16603-16611. https://doi.org/10.1016/j.ijhydene.2020.12.086

Flandroy, L., Poutahidis, T., Berg, G., Clarke, G., Dao, M.-C., Decaestecker, E., Furman, E., Haahtela, T., Massart, S., Plovier, H., Sanz, Y., & Rook, G. (2018). The impact of human activities and lifestyles on the interlinked microbiota and health of humans and of ecosystems. Science of The Total Environment, 627, 1018-1038. https://doi.org/10.1016/j.scitotenv.2018.01.288

Fu, C., & Jiang, M. (2019). Innovative methods to couple earth-abundant biomass waste with air batteries. Current Opinion in Electrochemistry, 15, 133-139. https://doi.org/10.1016/j.coelec.2019.04.029

Funke, A., Morgano, M. T., Dahmen, N., & Leibold, H. (2017). Experimental comparison of two bench scale units for fast and intermediate pyrolysis. Journal of Analytical and Applied Pyrolysis, 124, 504-514. https://doi.org/10.1016/j.jaap.2016.12.033

Fogassy, G., Thegarid, N., Toussaint, G., van Veen, A. C., Schuurman, Y., & Mirodatos, C. (2010). Biomass derived feedstock co-processing with vacuum gas oil for second-generation fuel production in FCC units. Applied Catalysis B: Environmental, 96, 476–485. https://doi.org/10.1016/j.apcatb.2010.03.008

Garcia-Nunez, J. A., Pelaez-Samaniego, M. R., Garcia-Perez, M. E., Fonts, I., Abrego, J., Westerhof, R. J. M., & Garcia-Perez, M. (2017). Historical Developments of Pyrolysis Reactors: A Review. Energy & Fuels, 31(6), 5751-5775. https://doi.org/10.1021/acs.energyfuels.7b00641

García Martín, J. F., Cuevas, M., Feng, C.-H., Álvarez Mateos, P., Torres Garcia, M., & Sánchez, S. (2020). Energetic valorisation of olive biomass: Olive-tree pruning, olive stones and pomaces. Processes, 8(5), 511. https://doi.org/10.3390/pr8050511

Ge, H., Zheng, J., & Xu, H. (2022). Advances in machine learning for high value-added applications of lignocellulosic biomass. Bioresource technology. https://doi.org/10.1016/j.biortech.2022.128481

Ghenai, C., Alamara, K., & Inayat, A. (2019). Solar assisted pyrolysis of plastic waste: pyrolysis oil characterization and grid-tied solar PV power system design. Energy Procedia, 159, 123-129. https://doi.org/10.1016/j.egypro.2018.12.029

Ghenai, C., Inayat, A., Shanableh, A., Al-Sarairah, E., & Janajreh, I. (2019). Combustion and emissions analysis of Spent Pot lining (SPL) as alternative fuel in cement industry. Science of The Total Environment, 684, 519-526. https://doi.org/10.1016/j.scitotenv.2019.05.157

Gholizadeh, M., Gunawan, R., Hu, X., de Miguel Mercader, F., Westerhof, R., Chaitwat, W., Hasan, M. M., Mourant, D., & Li, C.-Z. (2016). Effects of temperature on the hydrotreatment behaviour of pyrolysis bio-oil and coke formation in a continuous hydrotreatment reactor. Fuel Processing Technology, 148, 175-183. https://doi.org/10.1016/j.fuproc.2016.03.002

González, C. A. D., & Sandoval, L. P. (2020). Sustainability aspects of biomass gasification systems for small power generation. Renewable and Sustainable Energy Reviews, 134, 110180. https://doi.org/10.1016/j.rser.2020.110180

Hu, X., & Gholizadeh, M. (2019). Biomass pyrolysis: A review of the process development and challenges from initial researches up to the commercialisation stage. Journal of Energy Chemistry, 39, 109-143. https://doi.org/10.1016/j.jechem.2019.01.024

Hughey, C. A., Hendrickson, C. L., Rodgers, R. P., & Marshall, A. G. (2001). Elemental composition analysis of processed and unprocessed diesel fuel by electrospray ionization Fourier transform ion cyclotron resonance mass spectrometry. Energy & fuels, 15(5), 1186-1193. https://doi.org/10.1021/ef010088h

Jacobson, M. Z. (2009). Review of solutions to global warming, air pollution, and energy security. Energy & Environmental Science, 2(2), 148-173. https://doi.org/10.1039/b809990c

Jaswal, R., Shende, A., Nan, W., Amar, V., & Shende, R. (2019). Hydrothermal liquefaction and photocatalytic reforming of pinewood (Pinus ponderosa)-derived acid hydrolysis residue for hydrogen and bio-oil production. Energy & Fuels, 33(7), 6454-6462. https://doi.org/10.1021/acs.energyfuels.9b01071

Joardder, M. U. H., Halder, P., Rahim, M. A., & Paul, N. (2014). Solar assisted fast pyrolysis: A novel approach of renewable energy production. Journal of Engineering. https://doi.org/10.1155/2014/252848

Johnston, H. J., Mueller, W., Steinle, S., Vardoulakis, S., Tantrakarnapa, K., Loh, M., & Cherrie, J. W. (2019). How harmful is particulate matter emitted from biomass burning? A Thailand perspective. Current Pollution Reports, 5(4), 353-377. https://doi.org/10.1007/s40726-019-00125-4

James, J. J., Veethil, S. K., & Rajarathinam, J. R. J. (2022). Formulation and Evaluation of Topical Preparations Containing Pyrolytic Oil Obtained from Local Biomass. Indian Journal of Pharmaceutical Education and Research, 56(2s), s163-s170. https://doi.org/10.5530/ijper.56.2s.87

Kan, T., Strezov, V., & Evans, T. J. (2016). Lignocellulosic biomass pyrolysis: A review of product properties and effects of pyrolysis parameters. Renewable and Sustainable Energy Reviews, 57, 1126-1140. https://doi.org/10.1016/j.rser.2015.12.185

Kim, S., Tsang, Y. F., Kwon, E. E., Lin, K.-Y. A., & Lee, J. (2019). Recently developed methods to enhance stability of heterogeneous catalysts for conversion of biomass-derived feedstocks. Korean Journal of Chemical Engineering, 36, 1-11. https://doi.org/10.1007/s11814-018-0174-x

Kosinkova, J., Doshi, A., Maire, J., Ristovski, Z., Brown, R., & Rainey, T. J. (2015). Measuring the regional availability of biomass for biofuels and the potential for microalgae. Renewable and Sustainable Energy Reviews, 49, 1271-1285. https://doi.org/10.1016/j.rser.2015.04.084

Kumar, B., & Verma, P. (2020). Biomass-based biorefineries: An important architype towards a circular economy. Fuel, 288, 119622. https://doi.org/10.1016/j.fuel.2020.119622

Lee, H. W., Kim, Y. M., Jae, J., Sung, B. H., Jung, S. C., Kim, S. C., Jeon, J. K., & Park, Y. K. (2016). Catalytic pyrolysis of lignin using a two-stage fixed bed reactor comprised of in-situ natural zeolite and ex-situ HZSM-5. Journal of Analytical and Applied Pyrolysis, 122, 282-288. https://doi.org/10.1016/j.jaap.2016.09.015

Liu, Q., Liu, P., Xu, Z.-X., He, Z.-X., & Wang, Q. (2018). Bio-fuel oil characteristic of rice bran wax pyrolysis. Renewable energy, 119, 193-202. https://doi.org/10.1016/j.renene.2017.12.012

Liu, X., Burra, K. R. G., Wang, Z., Li, J., Che, D., & Gupta, A. K. (2021). Towards enhanced understanding of synergistic effects in co-pyrolysis of pinewood and polycarbonate. Applied Energy, 289, 116662. https://doi.org/10.1016/j.apenergy.2021.116662

Louwes, A. C., Basile, L., Yukananto, R., Bhagwandas, J. C., Bramer, E. A., & Brem, G. (2017). Torrefied biomass as feed for fast pyrolysis: An experimental study and chain analysis. Biomass and Bioenergy, 105, 116-126. https://doi.org/10.1016/j.biombioe.2017.06.009

Madhu, P., Stephen Livingston, T., & Manickam, I. N. (2017). Fixed bed pyrolysis of lemongrass (Cymbopogon flexuosus): Bio-oil production and characterization. Energy Sources, Part A: Recovery, Utilization, and Environmental Effects, 39(13), 1359-1368. https://doi.org/10.1080/15567036.2017.1328623

Maneffa, A., Priecel, P., & Lopez-Sanchez, J. A. (2016). Biomass-Derived Renewable Aromatics: Selective Routes and Outlook for p-Xylene Commercialisation. ChemSusChem, 9(19), 2736-2748. https://doi.org/10.1002/cssc.201600605

Mathimani, T., Baldinelli, A., Rajendran, K., Prabakar, D., Matheswaran, M., van Leeuwen, R. P., & Pugazhendhi, A. (2019). Review on cultivation and thermochemical conversion of microalgae to fuels and chemicals: Process evaluation and knowledge gaps. Journal of Cleaner Production, 208, 1053-1064. https://doi.org/10.1016/j.jclepro.2018.10.096

Gurevich Messina, L. I., Bonelli, P. R., & Cukierman, A. L. (2017). Effect of acid pretreatment and process temperature on characteristics and yields of pyrolysis products of peanut shells. Renewable Energy, 114, 697-707. https://doi.org/10.1016/j.renene.2017.07.065

Kaltschmitt, M. (Ed.). (2019). Energy from Organic Materials (Biomass). Springer New York. https://doi.org/10.1007/978-1-4939-7813-7

Miranda, N. T., Motta, I. L., Maciel Filho, R., & Maciel, M. R. W. (2021). Sugarcane bagasse pyrolysis: A review of operating conditions and products properties. Renewable and Sustainable Energy Reviews, 149, 111394. https://doi.org/10.1016/j.rser.2021.111394

Mirkouei, A., Haapala, K. R., Sessions, J., & Murthy, G. S. (2017). A review and future directions in techno-economic modeling and optimization of upstream forest biomass to bio-oil supply chains. Renewable and Sustainable Energy Reviews. https://doi.org/10.1016/j.rser.2016.08.053

Naushad, M., Sharma, G., & Alothman, Z. A. (2019). Photodegradation of toxic dye using Gum Arabic-crosslinked-poly(acrylamide)/Ni(OH)2/FeOOH nanocomposites hydrogel. Journal of Cleaner Production, 241, 118263. https://api.semanticscholar.org/CorpusID:203314092

Nagaraja, M., Kumar, R. D., Ashwanandhini, G., Nisha, V., Monika, L., Lakshmi, A. B., Sumitha, C., & Sivaranjani, E. (2013). Bio-energy from coconut shells. Advances in Agriculture, Sciences and Engineering Research, 3(2), 677-680. http://www.ejournal.sedinst.com/index.php/agser

Wang, Y., Li, X., Mourant, D., Gunawan, R., Zhang, S., & Li, C.-Z. (2012). Formation of aromatic structures during the pyrolysis of bio-oil. Energy & Fuels, 26(1), 241-247. https://doi.org/10.1021/ef201155e

Zhang B, et al. Fuel 2018;227:240–250.

Zhai, N., Mao, C., Feng, Y., Zhang, T., Xing, Z., Wang, Y., Zou, S., Yin, D., Han, X., Ren, G., & Yang, G. (2015). Current status and future potential of energy derived from Chinese agricultural land: a review. BioMed Research International. https://doi.org/10.1155/2015/824965

Shadangi, K. P., & Mohanty, K. (2014). Production and characterization of pyrolytic oil by catalytic pyrolysis of Niger seed. Fuel. https://doi.org/10.1016/j.fuel.2014.02.035

Figure 1: Collected coconut shells

Figure 2: Crushed coconut shells

Figure 3: FT-IR spectrum of the bio-oil

Figure 4: FT-IR spectrum of VGO

Figure 5: FT-IR spectrum of the Bio-oil

Figure 6: GC-MS spectra of the Bio-oil