Effect of calcination on the solubility of natural Tahoua phosphate in perchloric acid and in water

Abstract

The natural phosphate from Tahoua is a sedimentary phosphate containing a range of impurities. However, their presence in apatite makes phosphorus less available to plants. This work aims to enrich the natural phosphate from Tahoua to increase its solubility. In the first step, we carried out a heat treatment of the commercial phosphate from Tahoua. Calcination was performed in a kiln at 900°C for two hours. After treatment, we observed a loss of phosphate mass (from 8 g to 7.36 g). We then proceeded to chemically characterize the calcined phosphate by X-ray fluorescence spectrometry to determine the quantity of impurities removed from the phosphate's chemical composition. The results obtained were Al₂O₃ (from 4.64% to 0.485%), SiO₂ (from 3.35% to 0.05%), and P₂O₅ (from 20.6% to 30.8%). Finally, we dissolved the product obtained in perchloric acid and in water. The solubilization rates of calcined and merchant phosphate in perchloric acid and water were 58.75% and 16.30%, and 27.70% and 6.99%, respectively. Calcination of merchant phosphate significantly increased the concentration of P₂O₅ dissolved in both acid and water.

Keywords : Phosphate naturel, solubility, acid perchloric, water

- Introduction

Located in West Africa, Niger is a country rich in various raw materials, the majority of which have not yet been exploited industrially. It abounds in invaluable mineral resources, including iron, gold, uranium, limestone, tin, natron, phosphates, clays, etc. [1]. Furthermore, the population faces food insecurity due to climate change and soil degradation. To regenerate agricultural productivity, Niger's soil therefore requires the addition of certain nutrients, especially phosphorus, nitrogen, and potassium, which are fundamental to plant life. Of these three elements, phosphorus plays a crucial role in plant mineral nutrition [2]. In Niger, two natural phosphate deposits have been identified over the past several decades. The Tapoa natural phosphate deposit, with reserves estimated at 1.254 billion tonnes, and the Ader Doutchi deposit, estimated at 7,371,812 tonnes, are two examples of phosphate deposits. The latter was exploited by the Nigerien state through the National Office of Mining Research (ONAREM) and marketed by CAIMA (Central Supply of Agricultural Inputs and Materials), but the company's activities were suspended due to the product's low solubility [1]. Generally, Natural phosphate refers to naturally occurring mineral assemblages that contain a high concentration of phosphate minerals. The term encompasses both raw, unenriched phosphate ores and processed, concentrated phosphate products. Phosphate is commonly found as a sedimentary deposit in the form of apatite, a mineral with the general chemical formula Ca₅(PO₄)₃(F, OH, Cl), which may contain fluorine, hydroxyl, or chlorine ions. These deposits represent a primary source of phosphorus for agricultural and industrial applications [3].

The commercial phosphate from Tahoua is a nodular sedimentary phosphate composed primarily of fluoroapatite and has an average P2O5 content of approximately 30%. Its Fe2O3, Al2O3, SiO2, and organic matter content is too high, affecting the marketability of the nodules. Despite this percentage, approaches have been proposed to improve the solubility of natural phosphates, including acid etching for the production of superphosphates, combination with elemental sulfur, and biological solubilization [4]. Recent work has shown that natural phosphate from Tahoua can be transformed into simple superphosphate, an improved superphosphate, and that the reaction temperature strongly influences phosphate solubility.

However, Nigerien soils remain poor in phosphorus. To address this problem, numerous studies have been conducted on the use of natural phosphate from Tahoua in agriculture. Trials of direct application of commercial phosphate from Tahoua to agriculture have not yielded convincing results due to its low water solubility, resulting from its apatite form. Phosphorus from natural phosphate is only available to plants in an assimilable form [2]. It is an essential product for agriculture, just like nitrogen (N) and potassium (K), and is among the few non-substitutable raw materials [5]. In this case, natural phosphates contain impurities that negatively impact the product's quality. This justifie the need for processing to make it usable. This processing is carried out using physical and/or chemical methods (particle size analysis, water washing, flotation, separation, calcination, etc.). Thus, the calcination and the study of the solubility of natural phosphates from Tahoua (PNTs) in perchloric acid and in water were carried out.

- Materials and Methods

II.1. Materials

II.1.1. Phosphate Ore

Before being ready for processing, natural phosphate must undergo several treatment stages to obtain the desired quality. At the Tahoua mining complex, the treatments are geared towards producing a grade of phosphate suitable for market. In our research, we used market phosphate from Tahoua (Figure 1), purchased from the Central Supply Agency for Agricultural Inputs and Materials (CAIMA). The particle size of this powder ranges from 100 to 150 μm [4].

Figure 1: Merchantable phosphate powder from Tahoua

After heat treatment of the merchantable phosphate, we obtained a calcined product of a different color and with a lower mass than the initial product. The calcined phosphate is shown in Figure 2.

Figure 2: Calcined Tahoua phosphate powder

II.1.2. Chemicals

The chemicals used in this work are described in the table below.

Table 1: The chemicals used for this work

| Produits | Formule | Masse molaire g/mol | Densité | Pureté | Origine |
| --- | --- | --- | --- | --- | --- |
| Acide sulfurique | H2SO4 | 98 | 1,84 | 95̶̶ 98% | Prolabo̶Normapur |
| Acide citrique | C6H807 H2O | 210,124 | 1,55 | 100% | ProlaboNormapur |
| Molybdate d’ammonium | NH4M07. 4H2O | 1235,86 | _ | _ | ACROS ORGANICS |
| Tartrate de potassium et antimoine | C4H4O6 K(SbO).0, 05H2O | 333,93 | 2,6 | 99% | ACROS ORGANICS |
| Acide ascorbique | C6H806 | 176,13 | _ | 99,7% | ProlaboNormapur |
| Phosphate mono potassique | KH2PO4 | 136,1 | _ | _ | _ |

II.1.3. Equipment

The equipment used in our work included:

▪ a molecular absorption spectrophotometer;

▪ an analytical balance ;

▪ filtrate collection bottles;

▪ magnetic stirrers;

▪ a hot plate ;

▪ certain laboratory equipment (volumetric flasks, pipettes, funnel, wash bottle);

▪ filter paper;

▪ an X-ray fluorescence spectrometer

II.2. Methods

II.2.1. Enrichment of Tahoua Natural Phosphate by Calcination

An 8 g mass of Tahoua natural phosphate powder, weighed using a precision balance, was placed in a crucible. It was then placed in a furnace at the calcination temperature of 900 °C for 2 hours. Then it is left to cool in the oven for 24 hours and collected in a dry container. This type of calcination burns off the organic matter without significantly affecting the superior qualities of the sedimentary phosphates.

II.2.2. Principles of X-ray Spectrometry

X-ray fluorescence (XRF) is an analytical technique employed to determine the elemental composition of solid samples. In this method, X-rays are used to excite the atoms within the sample, causing them to emit secondary X-rays with energies characteristic of the specific elements present. As a quantitative analytical tool, XRF allows for precise measurement of elemental concentrations based on the energy and intensity of the emitted radiation. The technique operates according to the principles of electromagnetic radiation, whereby a material can absorb incident X-rays and subsequently re-emit them, providing information about its elemental composition.

The generation of X-rays originates from the energy loss that occurs when high-energy electrons interact with atoms. Electrons emitted from the X-ray tube are directed towards the electron cloud of atoms in the target material, where they are decelerated and lose energy. Some high-energy incident electrons penetrate the outer electron shells and collide with inner-shell electrons, which may be ejected entirely, leaving the atom in an excited, unstable state. To restore stability, electrons from higher energy levels rearrange to fill the vacancies in the inner shells, and the energy released during this process is emitted as X-rays. The resulting X-rays possess discrete wavelengths specific to the atomic number of the target atoms and are referred to as “characteristic X-rays.” The detection and quantification of these characteristic X-rays form the fundamental principle of X-ray spectrometry, enabling precise elemental analysis [7].

Chemical analysis was performed on 20 g of crude powder using an energy-dispersive X-ray fluorescence spectrometer (Minipal 4 model). Kapton filters were selected for major oxides, and Ag/Al-thin filters were used for trace elements and rare earth elements. The measurement for each sample was conducted over a duration of 100 seconds, with air consistently employed as the measurement medium. Loss on ignition (LOI) was determined using a gravimetric approach, whereby 1 g of finely powdered sample was placed in a pre-weighed, clean crucible and subjected to heating at 1000 °C. Following combustion, the crucible and its residual contents were reweighed, and the difference in mass before and after heating was used to calculate the LOI. This procedure provides a reliable estimate of the volatile and combustible components in the sample, which is essential for characterising its mineral and organic content.

LOI = (a-b) x 100%

Where a = weight of crucible + sample before heating

b = weight of crucible + sample after heating.

Figure 3: X-ray fluorescence spectrometer [7]

II.1.3.1. Determination of total P2O5 (P2O5 T)

A 0.50 g mass of the simple superphosphate fertilizer, weighed using a precision balance (Precisa 205 A type), is placed in a previously washed and dried 250 mL beaker. A few mL of distilled water are added, along with 7.5 mL of perchloric acid. The mixture is heated until all the white coloration disappears on a plate. After cooling, the contents are transferred quantitatively into a 250 mL volumetric flask, after thoroughly rinsing the beaker with distilled water. The mixture is homogenized, and the volume is then filled to the mark on the calibration cylinder. The resulting mixture is filtered through pleated filter paper, discarding the first few mL of the filtrate into a dry flask. Finally, the concentration of dissolved phosphoric anhydride (P₂O₅) was determined in the filtrate [8].

II.1.3.1. Determination of Water-Soluble P₂O₅ (P₂O₅ SE)

In a 250 mL flask, previously rinsed thoroughly with distilled water, 0.25 g of simple superphosphate fertilizer was added along with 100 mL of distilled water. The resulting suspension was agitated using a magnetic stirrer at room temperature, with the stirring speed maintained at 500 rpm for a total reaction time of 20 minutes. Following agitation, the mixture was filtered through rapid filter paper, and the filtrate was collected in a clean, dry plastic bottle, discarding the initial few millilitres to avoid contamination. The concentration of dissolved phosphoric anhydride (P₂O₅) in the filtrate was subsequently determined to evaluate the solubilising effect of water on the simple superphosphate. To ensure the accuracy and reproducibility of the results, the entire procedure was repeated in triplicate.

II.1.3.3. Preparation of the Complexing Solution

The phosphate ions released during the reaction were subjected to complexation using a designated complexing solution. The preparation of this solution involved the careful formulation of three separate solutions in equal proportions, which were subsequently combined in a specific sequential order [8]. The solutions are prepared as follows:

Solution 1: a 250 mL solution was prepared, consisting of one volume of nitric acid and two volumes of distilled water;

Solution 2: 0.625 g of ammonium metavanadate (NH4VO3) was dissolved in a 250 mL volumetric flask with 150 mL of boiling distilled water. After stirring, 5 mL of nitric acid (HNO3, d = 1.38) was added. The volume was then made up to the mark with distilled water after cooling;

Solution 3: A mass of 12.5g of ammonium molybdate tetrahydrate Mo7O24(NH4)6 4H2O is dissolved in 200 mL of boiling distilled water and the volume is made up to 250 mL with distilled water.

III. Results and Discussion

III.1. Processing of Tahoua Merchant Phosphate

The enrichment of natural phosphate by calcination is a means of removing impurities from the raw phosphate, namely water and organic matter. This increases the phosphate (P2O5) content in the ore. The variation in mass obtained by calcining the ore is shown in Table 2:

Table 2 : Masses of Raw and Calcined Natural Phosphate from Tahoua

|  | Merchand phosphate | Calcined phosphate |
| --- | --- | --- |
| Masses in g | 8 | 7,36 |

After heat treatment of the raw phosphate, the results show a decrease in phosphate mass. This mass loss can be attributed to the removal of impurities such as organic matter, water, etc. This removal could contribute to an increase in the P2O5 content of the phosphate. In this regard, El Ouardi and his colleagues [9] observed a mass loss and an increase in P2O5 content in the calcined phosphate.

III.2. Determination of the Chemical Composition of Calcined Phosphate by X-ray Fluorescence

Three samples of raw phosphate and two samples of calcined phosphate were analyzed by energy-dispersive X-ray fluorescence spectrometry (EDXRF) using the Minipal 4 model, but only the average of the results is presented in Table 3.

Table 3 : Chemical Composition of Raw and Calcined Phosphate

| Major eléments in % |  |  |  | Trace elements in ppm |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Oxides | Crud Phosphate | Calcined Phosphate |  | Métals | Crud Phosphate | Calcined Phosphate |
| CaO | 53,18 | 51,13 |  | Sr | 4579,02 | 3191,69 |
| P2O5 | 20,6 | 30,8 |  | Sc | 41,667 | 212,18 |
| Fe2O3 | 9,89 | 14,88 |  | Nb | 39,967 | 150,73 |
| Al2O3 | 4,64 | 0,485 |  | Ba | - | 501,52 |
| SiO2 | 3,35 | 0,051 |  | Cu | 219,68 | 60,23 |
| MnO | 0,931 | 0,751 |  | Zr | 301,96 | 200 |
| MgO | 0,763 | 0,015 |  | Zn | 8,246 | 5,03 |
| TiO2 | 0,346 | 0,2 |  | Bi | - | 28,5 |
| Na2O | 0,081 | <0,001 |  | Hg | - | 3,869 |
| K2O | 0,048 | <0,001 |  | La | - | 0,48 |
| LOI (loss in ignition) | 5,2 | 1,1 |  | Hf | 24,06 | 41,465 |
|  |  |  |  | Pb | <0,01 | 225 |
|  |  |  |  | Y | - | 21,25 |
|  |  |  |  | V | 9,976 | - |
|  |  |  |  | As | 14,056 | - |
|  |  |  |  | W | 0,626 | - |
|  |  |  |  | Ta | 12,016 | - |

The results obtained before and after heat treatment are respectively: for P2O5 (from 20.6% to 30.8%), for Al2O3 (from 4.64% to 0.485%), for SiO2 (from 3.35% to 0.051%), and for MgO (from 0.763% to 0.015%). We observe an increase in the P2O5 content of calcined phosphate and a decrease in certain impurities such as Al2O3, SiO2, and MgO. This can be explained by the removal of large portion of impurities such as organic matter, silica, water, aluminum oxide, and magnesium oxide. In other studies, authors have shown that impurities do not promote phosphate valorization processes and their effectiveness in direct agricultural application [10, 11]. Similarly, Mr. El Ouardi and his colleagues [9] showed that the P2O5 content increases and the impurity content decreases at a temperature of 850°C for 30 minutes. Removing the impurities does not affect the P2O5 content. It is important to note that the presence of organic matter and oxides in marketable phosphate affects its valorization and solubility.

III.2. Solubility of Natural Phosphate from Tahoua in Solutions

Tradeable phosphate from Tahoua is a sedimentary phosphate [1]. It is mainly composed of fluoroapatite. The decomposition of fluoroapatite takes place at the surface of the solid substrate and proceeds as a chemical reaction that does not require a catalyst. During the dissolution process, bond cleavage occurs sequentially, beginning with the weakest bonds and progressing towards the strongest. Accordingly, the dissolution of fluoroapatite is initiated by the cleavage of Ca–F bonds, followed by Ca–P bonds. In contrast, the P–O bonds, which possess the highest bond energies, remain intact, thereby preserving the overall structural framework [12]. In acidic media, the phosphate, in the form of PO43- ions, binds H+ ions to form HPO42- or H2PO4- ions, depending on the strength of the acid. The decomposition reaction of fluoroapatites in acidic solutions can be written [13]:

Ca10(PO4)6F2 + 14H+ → 10Ca2+ + 6H2PO4- + 2HF

We studied the dissolution of the ores in perchloric acid and water. This was evaluated by measuring the P2O5 content in the different filtrates collected after treatment. We will present and discuss the results of this study in the following paragraphs.

III.2.1. Solubility of PMT and Calcined Phosphate in Perchloric Acid Solution

The dissolution of natural phosphates from Tahoua (PMT and PMC) in perchloric acid solution was carried out. The results obtained are presented in Figure 4. It shows the total P2O5 content in the marketable and calcined phosphate.

Figure 4 Dissolved P2O5 content in perchloric acid

Analysis of these results shows that the percentage of dissolved P2O5 in calcined phosphate (58.75%) is double that of raw phosphate (27.70%). This increase in the dissolved P2O5 content of calcined phosphate can be explained by the increase in the specific surface area of ​​phosphate, according to FAO [14], and by the release of phosphate particles and the destruction of organic matter. D. Akila and F. Zahia [15] showed that the rise in P2O5 content is due to the release of phosphate particles after the destruction of carbonates and organic matter by thermal effect. This results in significant consumption of H3O+ ions in the medium, increasing the dissolution of ores [16]. The solubilization rates we obtained after calcination are higher than those obtained [16, 17, 18] for the dissolution of Tahoua merchant phosphate, natural phosphate from Togo, and natural phosphate from Algeria [19].

III.2.2. Solubility of Calcined Phosphate (CP) and Tahoua Merchant Phosphate (PMT) in Water

The determination of phosphoric anhydride in the filtrates obtained from the treatment of calcined and merchant phosphate with distilled water yielded the results shown in Figure 5.

Figure 5 : Water-soluble P2O5 content

These results show that the dissolved P2O5 content of calcined phosphate (16.30%) is almost twice that of commercial phosphate from Tahoua (6.99%) in water. This reveals that heat treatment has a major impact on the release of soluble phosphates. Calcination appears to promote the transformation of less soluble phosphate forms into more reactive and bioavailable forms. This increase in dissolution could be attributed to the effect of heat treatment, i.e., the removal of impurities, particularly organic matter, water, aluminum oxide, iron oxide, and free phosphate ions, promotes the dissolution of calcined phosphate in water. Our results are consistent with the work carried out by Bassirou I on the comparative study of the dissolution of natural phosphate from Tahoua in various mineral and organic acids [16].

III.2.3. Comparative Study of the Dissolution of Phosphates (Calcined and Merchant) by Perchloric Acid Solution and Water

To better understand the differences and similarities in the reaction processes of apatite with perchloric acid and water, we conducted a comparative study of the dissolution rates of merchant and calcined phosphates by perchloric acid solution and water. The dissolution rates of calcined and raw phosphates in the two solutions are shown in Figure 6.

Figure 6 : Comparison of the P2O5 Dissolution Rate in Perchloric Acid Solution and Water

Based on these results, the dissolution rates of calcined phosphate and merchantable phosphate in perchloric acid and water solutions show a notable difference, with the perchloric acid solution exhibiting the highest dissolution rate. The dissolution rates of calcined phosphate were only 58.75% and 16.30%, and for merchantable phosphate, 27.70% and 6.99%, respectively, in perchloric acid and water solutions. These results indicate that phosphate dissolution is not complete, confirming the difficulty in fully dissolving certain natural phosphates. This can be explained by the presence of residual impurities in the ores, such as SiO2, Fe2O3, and Al2O3, which hinder dissolution. Furthermore, dissolution is generally slow and depends on the ability of phosphate ions to release themselves from mineral structures in water, while dissolution is rapid and also depends on hydronium ions, which facilitate the decomposition of phosphate structures, releasing phosphate ions into the solution. Previous work has shown that dissolution depends on the destruction of carbonates and organic matter by thermal effect to release phosphate particles [15]. In this sense, the work of Alexandra Jourdan has shown that the dissolution of this dolomitic material, of variable hygrometry, was slow [20].

Conclusion

In this study, we performed calcination at 900°C for 2 hours. At the end of the process, a decrease in the mass of the phosphate sample was observed. Characterization of the calcined and raw phosphate using X-ray fluorescence spectrometry showed that the P₂O₅ content increased from 20.6% in the raw phosphate to 30.8% after calcination, representing a 10.2% increase. We then studied the dissolution of the commercial and calcined phosphate in perchloric acid and water. The results of the dissolved phosphorus analysis, expressed as a percentage of phosphoric anhydride (P₂O₅), showed that the calcined phosphate dissolves more readily and that dissolution is greater in perchloric acid than in water.

Disclainer(Artifical Intelligence)

Author(s) hereby declare that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc) and text-to-image generators have been used during writing or editing of this manuscript.

References

- Franconi, A., Julien, J., and Zibo, I. (1980). Mineral Map of the Republic of Niger, Volume IV, Part 1. Specific study of the main mineral substances and their geological context, 725 pp. Faculty project no. 259/CD/80 and 383/CD/81.

- Zanguina, A. (2011). Contribution to the physicochemical characterization and agronomic development of natural phosphate from Tahoua (Niger): Trials for the production of certain mineral fertilizers and phospho-compost. Doctoral thesis in Physical Chemistry of Materials, Abdou Moumouni University of Niamey, 149 pp.

- Boujier, V. (2007). Influence of monohydrogen phosphate and fluorophosphate ions on the properties of phosphogypsum and the reactivity of phosphoplating. Doctoral thesis in Process Engineering. National School of Mines of Saint-Etienne

- Zapata, F. and R.N. Roy, (2004). Use of natural phosphates for sustainable agriculture. FAO Bulletin Fertilizers and Plant Nutrition No. 13 ISSN 0259-6180, 176

- Akila, D., Zahia, F., (2016). The influence of heat treatment on the particle size distribution of beige phosphate ore from the Kef Es Sannoun Djebel Onk deposit. Master's thesis in mineral resource valorization. Abderrahmane Mira University of Bejaia

- Natatou, I., A. Maman, A. Zanguina, I. Khalid, A. Boos and M. Burgard, (2004). Physico-chemical studies of marketable phosphate from Tahoua (Niger). J. Soc. Ouest-Afr. Chim.; 018; p. 137-148.

- Willis, Ken Turner and Gary Pritchard, (2011). XRF in the workplace: A Guide to Practical XRF Spectrometry. https://catalogue.nla.gov.au/catalog/5755969.

- Achraf El Hallaoui 1,*, Tourya Ghailane, Soukaina Chehab 1, Youssef Merroun 1, Rachida Ghailane 1, Said Boukhris 1, Taoufik Guédira 1 and Abdelaziz Souizi 1,* (2021)., Synthesis of new bimetallic phosphate (Al/Ag3PO4) and study for its Catalytic performance in the synthesis of 1,2-dihydro-l-phenyl-3H-naphth [1,2-e]-[1,3] oxazin-3-one derivatives. DOI: http://dx.doi.org/10.13171/mjc02108091579elhallaoui

- El Ouardi, M., Mrani, I., Anoua, M., & Chehouani, H. (2009). Optimization of the thermal treatment of a phosphate: application to phosphate from the Gantour basin in Morocco. Materials & Techniques, 97(2), 133-142, https://doi.org/10.1051/mattech/2009014.

- Cuney, M. (2004). “Factors controlling the nature and concentration of impurities in sedimentary phosphates”, COVAPHOS I (ed), Proceedings of the first international conference on the valorization of phosphates and phosphorus compounds, pp. 11-14.

- United Nations Industrial Development Organization (UNIDO) & IFDC, (1998). Fertilizer manual. Dordrecht, the Netherlands, Kluwer Academic Publishers, p. 615.

- Claire Chairat, (2005). Experimental study of the kinetics and alteration mechanisms of apatitic minerals. Application to the behavior of a minor actinide confinement ceramic. Doctoral thesis, University of Toulouse III, in experimental geochemistry.

- Valyasko, V. M., Kogardo, L. N., Khodakovsky, I. L. (1968). Stability of fluorapatite, chloroapatite and hydroxylapatite in aqueous solutions at different temperatures. Goech. Inter., 5, p. 21-30.

- Food and Agriculture Organization of the United Nations (FAO, 2013). Use of natural phosphates for sustainable agriculture. FAO Fertilizers and Plant Nutrition Bulletin. Mining of natural phosphates in Khouribga, Morocco.

- Akila, D., Zahia, F. (2016). The influence of heat treatment on the particle size distribution of beige phosphate ore from the Kef Es Sannoun Djebel Onk deposit. Master's thesis in mineral resource valorization. Abderrahmane Mira University, Bejaia.

- Bassirou, I., Halidou (2015). Comparative study of the dissolution of natural phosphate from Tahoua in various mineral and organic acids. Master's thesis in inorganic chemistry, Abdou Moumouni University of Niamey, 60 pp.

- Zanguina, A. (2011). Contribution to the physicochemical characterization and agronomic development of natural phosphate from Tahoua (Niger): Trials for the production of certain mineral fertilizers and phospho-compost. Doctoral thesis in Physical Chemistry of Materials, Abdou Moumouni University of Niamey, 149 p.

- Ousmane M. S., (2018). Physicochemical characterizations, improvement of agronomic efficiency by phosphocomposting of natural phosphates from Niger. Doctoral thesis in Applied Sciences, Abdou Moumouni University of Niamey, 116 p.

- Lassis, M., A. Mizane, N. Dadda, R. Rehamnia, (2015). Dissolution of Djebel Onk phosphate ore using sulfuric acid. ENMM-20; No., p.

- Alexandra Jourdain (2023). Study of the physicochemical properties of lamellar double hydroxides for the controlled release of phosphate as a fertilizer. Materials. Clermont Auvergne University. French. NNT: 2023UCFA0028.