POTENTIAL OF USE OF PFAFFIA GLOMERATA (BRAZILIAN GINSENG) IN THE GREEN SYNTHESIS OF METALLIC NANOPARTICLES: REVIEW STUDY

Abstract

The synthesis of metallic nanoparticles using plant extracts has shown great interest in the scientific community, due to the special properties that can be applied to various fields of science such as health, agronomy, and food. The bioreduction or green synthesis can be performed using plant extracts that have alkaloids, phenolic compounds, terpenoids, enzymes, proteins, amino acids, polysaccharides, and functional groups, that are responsible for reducing metal ions. However, the antimicrobial effect of silver and gold nanoparticles synthesized using plant extracts has not been fully elucidated. This study aimed to conduct a literature review on "nanoparticles," "green synthesis," "plants ginseng," and "antimicrobial" in major scientific databases from 2013 to 2023. The results of the reviewed studies demonstrated the use of Panax ginseng, Siberian ginseng, and red and black ginseng in the synthesis of silver and gold nanoparticles, with potential applications as antimicrobials and anticancer agents. In conclusion, it is essential to conduct further research on the studied plant species, particularly those belonging to the Amaranthaceae family, to deepen our understanding of the mechanisms and reducing agents involved in the green synthesis of silver and gold nanoparticles.

Keywords: Plant extracts, Sustainability, Bacteria, Green chemistry, Ginseng brasileiro.

1 Introduction

The excessive and incorrect use of antibiotics over an extended period induces microbial resistance, being the cause of infections in the community, encompassing a wide range of pathogens in humans. This has contributed to the emergence of drug-resistant bacteria, sometimes resulting in the ineffectiveness of commercial antibiotics. An alternative would be the use of natural products such as medicinal plants, plant extracts, and essential oils that contain bioactive compounds. These substances have been studied for their ability to inhibit the growth or cause the death of microbial agents. This scenario highlights the need for continuous exploration of discoveries and scientific studies in the chemical and medicinal fields. The field of nanotechnology has been gaining prominence in various areas of knowledge due to its unique physicochemical properties (distinct from those presented by their counterparts on a macroscopic scale) and surface interaction mechanisms. In this context, metallic nanoparticles, which are small aggregates of metals on a nanoscale, hold significant potential for applications in environmental, agricultural, health, and food-related fields (Saravanan et al., 2021; Abisharani et al., 2019; Wongyai et al., 2020; Kalita; Baruah, 2019).

Over the years, various synthetic methods have been studied for obtaining metallic nanoparticles through physical, chemical, and photochemical means (Yagoob et al., 2020). However, most available techniques are expensive and environmentally unfriendly, meaning they can be harmful to the environment. The green synthesis of metallic nanoparticles offers significant advantages in production compared to traditional methods (Baláž et al., 2021). This approach utilizes renewable materials such as plants, fungi, algae, and bacteria as reducing and/or stabilizing agents, avoiding the use of toxic substances and reducing waste production. Inserido neste contexto, destaca-se o ginseng (dentre as variadas 11 espécies conhecidas), que ajuda no sistema imunológico, é antioxidante e ainda possui outras finalidades funcionais (Wang et al., 2020).

Therefore, the objective of this work is to present a literature review on sustainable methods for the green synthesis of metallic nanoparticles, specifically gold and silver, using extracts from ginseng species.

2. State of the art

2.2 Ginseng

There are several species of ginseng found throughout the world. They are of medicinal interest, particularly in Asian countries such as China and Japan. Among the main species are: a) Panax ginseng, known as Korean ginseng, found in China and Korea; b) Panax japonicus (Mohsin et al., 2020), known as Japanese ginseng, found in Japan and China; c) Panax quinquefolius or American ginseng, found in the United States and Canada; d) Eleutherococcus senticosus (Gerontakos et al., 2021), popularly known as Siberian ginseng, found in Russia; e) Pfaffia glomerata or Brazilian ginseng, found in Brazil.  In each of these species, various bioactive compounds with antioxidant, anti-inflammatory, anti-diabetic, antimicrobial, and other properties can be found.

2.2.1 Ginseng brasileiro (Pfaffia glomerata)

Pfaffia glomerata (Spreng.) Pedersen is one of the three species in the Pfaffia genus, belonging to the Amaranthaceae family. Indigenous to South American countries, particularly in Brazil, in regions spanning Paraná, São Paulo, Goiás, and Mato Grosso, Pfaffia glomerata is commonly referred to as Brazilian ginseng. This nomenclature stems from both its morphological resemblance to Asian ginseng and its similar medicinal effects. (Vardanega et al., 2016, Huang et al., 2021).

In Brazil, Pfaffia glomerata grows endemically near rivers due to the soil composition and the existing moisture. In the state of Paraná, the municipality of Querência do Norte is one of the major producers. The cultivation in this area is carried out sustainably by the inhabitants of the Ilha Grande National Park.

Present in Pfaffia glomerata, the component β-ecdysone (20E) or 20-hydroxyecdysone is a phytoecdysteroid that is analogous to insect hormones. The extraction of secondary metabolites from Pfaffia glomerata is crucial in the discovery of new constituents. (Balastreri et al., 2018). Due to its significant presence in Pfaffia glomerata, β-ecdysone is considered the chemical marker of this plant. (Neves et al., 2016). Martins et al. (2020) detected the presence of β-ecdysone in the roots, stem, flowers, and leaves (0.68 ± 0.05, 0.62 ± 0.06, 1.14 ± 0.10, and 1.65 ± 0.14, respectively) in Pfaffia glomerata harvested in the Paraná River basin. In addition to this compound, the authors reported increasing total phenolic content in the order: leaf > flower > stem > root. In the leaf, chlorogenic, ferulic, and hydroxybenzoic acids are present (Martins, 2020).

2.3 Green synthesis of metallic nanoparticles

The concept of nanotechnology involves physics, medicine, chemistry, biology, and materials science. The prefix "nano" is derived from the Greek word "nanos," meaning dwarf. In engineering terms, it represents one billionth of size, that is (10-9m), with a nanometer considered in the order of <100 nm. For instance, a protein has an approximate length of 50 nm. Nano-scale materials are of interest because they can be produced in different forms. However, it is crucial to be able to produce them in a reduced timeframe and at the desired size to enhance their stability (Hulkoti; Taranath, 2014). In general, nanoparticles have an approximate size of up to 100 nm and a large surface area about their volume. Due to these characteristics, nanoparticles are of great scientific interest, as they can be used, for example, to traverse cell membranes or biological barriers. Therefore, the size reduction of nanoparticles has offered significant possibilities for scientific advancements in modern technology, with enormous potential for the well-being of humans (Balakumaran et al., 2015).

The chemical, physical, and photochemical methods are the most common for the synthesis of metallic nanoparticles (NPMs). (Yaqoob et al. 2020). The chemical routes commonly used for the synthesis of metallic nanoparticles (NPs) often involve the use of toxic solvents and the subsequent generation of environmentally harmful waste (Silva et al. 2017).

The metals commonly used to form metallic nanoparticles (NPs) include gold, silver, zinc, copper, iron, platinum, aluminum, titanium, and palladium. The mechanisms for these syntheses have not been completely elucidated due to the complexity of the reaction medium, as additional reducing agents (sodium borohydride, hydrazine) can be used, as well as other nanoparticle stabilizers. Their properties involve photoelectrochemical, magnetic, and electronic aspects. Infrared spectroscopy data have revealed that the bands corresponding to amino groups, present in proteins, are responsible for stabilizing the particles, preventing the growth of nanoparticles (NPs). (Hulkoti; Taranath, 2014).

The change in solution color to brown indicates the formation of AgNPs (silver nanoparticles). In the research area, for proper characterization of nanoparticles, it is necessary to monitor their size, morphology, and shape through stabilization and various types of reducing agents. Green synthesis gains prominence due to its cost-effectiveness, flexibility, and ease of preparation (Deshmukh; Gupta; KIM, 2019). Barabadi et al. (2014) indicate that during the formation process of AuNPs (gold nanoparticles), a color change from pale yellow to dark purple occurs, attributed to the emergence of the surface plasmon band. This band occurs on small metallic surfaces due to the collective oscillation of surface electrons interacting with incident monochromatic radiation. Thus, an electronic transition in the visible spectrum region occurs, indicating the formation of the metallic nanoparticle. In Figure 1, a scheme of the NPs' role in intracellular synthesis is described.

Figure 1. Representation of intracellular synthesis of a nanoparticle. N-nucleus, NP-nanoparticle, (+) ions, (-) charges on the cell wall. Source: Authors, 2023. (https://Biorender.com)

Due to the growing concern for the development of cleaner and more sustainable technologies, efforts have been made to develop metallic nanoparticle (NPM) synthesis technologies using non-toxic or less toxic reagents and solvents, as well as renewable sources, with reduced waste generation, among other aspects. Rai (2013) highlights that, in addition to these aspects, green synthesis should also be clean, cost-effective, and environmentally friendly. Green synthesis primarily employs fungi, bacteria, and plant extracts for the reduction and stabilization of nanoparticles (NPs). An advantage of using plant extracts is that they can act in the synthesis in three ways, primarily reducing silver or gold ions, metals more commonly employed in this type of synthesis. This is because these matrices contain aldehydes, ketones, and carboxylic acids in their composition, accelerating the generation of metallic nanoparticles more rapidly. Another contribution of the extracts lies in promoting the stability of the nanoparticles, eliminating the need for reagents that would bind to the surface to prevent agglomeration and precipitation of the material. The antimicrobial activity observed in metallic nanoparticles (NPMs) from plant extracts primarily arises from the quantity of silver or another metal released, which interacts with fluids and the sample's water (Behravan et al., 2018). However, depending on the plant species employed, there may be an enhancement or synergy in the antimicrobial action due to the combination with the metal of the nanoparticle.

The synthesis of these metallic nanoparticles (NPM) is of interest in biomedicine, optics, catalysis, and photonics. Gold NPMs, due to their stability under atmospheric conditions and oxidation resistance, find application in pharmaceuticals. Their average diameter is influenced by the pH of the medium, salt concentration, and incubation temperature. The condition for the green synthesis of AgNPs and AuNPs involves having a biological agent for reduction, which is abundantly found in biological systems. Initially, silver ions are acquired from water-soluble salts, with water being the most preferable solvent. (Srikar et al., 2016).

Parte superior do formulário

The mechanism of AgNPs synthesis occurs through the reduction of silver nitrate, where the substitution is carried out by bioorganic compounds, playing a significant role in their antifungal and antimicrobial performance. Nanoparticles tend to aggregate to reduce surface energy, which diminishes their antibacterial effectiveness. (Qasim et al., 2015).

In the synthesis of AgNPs, the silver ion (Ag+) is derived from the silver salt, such as nitrate, which, in an aqueous medium, becomes reactive and can form other compounds. Silver nitrate is a salt with antimicrobial activity. An NP, on the other hand, is an agglomeration of reduced silver atoms. Metallic nanoparticles (NPMs) with a precursor salt containing the metal stabilize the suspension. Their color intensities vary depending on the concentration of the salt combined with the plant extract in use. The size of the NP can also interfere with the antimicrobial effect. Silver nitrate acts internally within the cell, while NPs act on the cell membrane, causing its rupture (Porto, 2012).

According to Carmona et al. (2017), the green synthesis of silver nanoparticles involves the chemical reduction of silver from the AgNO3 solution and the use of a plant extract, where nucleation occurs, and silver atoms, along with high activation energy, form small nuclei. The phase in which these nuclei are grouped (giving rise to AgNPs) can be stable in their creation. The choice of the selected extract is ideal because the biomolecules present provide the reducing agents in the synthesis. Figure 2 illustrates the mechanism that occurs in green synthesis with plant extracts. The plant extract is added to the metallic salt under constant temperature and agitation. After a change in the color of the solution, the steps of solid formation, nucleation, and the growth of small particles take place, ultimately resulting in the formation of NPMs in different shapes.

Figure 2. Green synthesis procedure for the formation of metallic nanoparticles. Source: Authors, 2023. (https://Biorender.com)

Several factors, such as the type of extract, concentration of the metallic salt, pH, and synthesis temperature, can influence the synthesis time and morphology of NPMs. Therefore, there is a greater consumption of reagents, energy, and working time. An advantage of green synthesis is that it usually does not require additional stabilizing additives, which is a positive aspect compared to chemical methods (Barabadi et al., 2014).Parte superior do formulário

Carmona et al. (2017) reported in their study the use of Buddleja globosa Hope, where they used 5% of the plant extract volume added to AgNO3 with a variation of 0.1 to 10 mmol/L to synthesize AgNPs. They mentioned that phenolic compounds, terpenoids, proteins, amino acids, enzymes, flavonoids, polysaccharides, and alkaloids are compounds that can contribute to green synthesis.

The study by Sathishkumar et al. (2016) demonstrates that flavonoids found in cut leaves of Alternanthera tenella stimulate the synthesis of AgNPs. For Chysanthemum indicum, glycosides, tannins, and flavonoids were responsible for the formation, according to the author. In the case of Potentilla fulgens, flavonoids were four times more responsible for nanoparticle formation than phenolics. For European black elderberry, carbonyl and hydroxyl groups derived from the extract showed the reduction of ions into metallic silver. Other flavonoids such as hesperidin, diosmin, and naringin resulted in NPs ranging between 5-80 nm in size.

To Siakavella et al. (2020), the biological basis of synthesis using plant extracts is considered the best method. Since 1900, the characteristic of these materials in reducing metal ions and also acting as stabilizing agents has been known. This prevents particles from aggregating in the plant extract. Different reports indicate the preparation conditions; thus, it is valid to observe the impact of each extract on the preparation of NPs. Finally, Rajan et al.'s study (2018) conducted synthesis using henna leaves (Lawsonia inermis) with cadmium chloride and selenium (done separately). After 1 minute, the light yellow color turned brown, indicating a reaction that remained stable for over 2 days without alteration. One possible explanation for the synthesis was provided through the secondary metabolites present in the green extract.

According to Barabadi et al. (2014), in a study conducted with species of the fungus Penicillium and bacteria from the Enterobacteriaceae family, the biological synthesis of nanoparticles was carried out using copper oxide, silver, and gold.

2.1 Microorganisms of interest

Bacteria and fungi are microorganisms that belong to the Monera and Fungi kingdoms, respectively. The former can be found in the environment, and the human body, and some can cause diseases. Fungi, on the other hand, are also commonly found in nature, and some fungi, such as the one causing candidiasis, can be harmful to humans. The treatment of certain bacteria, such as Staphylococcus aureus, results in a high cost to the healthcare system due to the potential need for prolonged antibiotic use. Currently, some microorganisms have developed resistance to most antimicrobials available on the market, including oxacillin, methicillin, cephalosporins, and others. This resistance poses a significant threat to global health. On the other hand, the exploration and study of nanoparticles, which exert toxicity to bacteria through mechanisms similar to conventional antibiotics, can be an alternative in treatment. Examples of this include silver nanoparticles (AgNPs): they disrupt cellular morphology, hinder ribosome interaction, deactivate proteins, and accumulate a lethal amount within the cell (Jankauskaite et al., 2016).

According to Correa et al. (2020), one of the most significant microorganisms causing hospital, urinary, and intestinal infections is Escherichia coli (E. coli). It is a Gram-negative, facultative anaerobic bacterium that is a natural part of the human intestinal microbiota. This bacterium affects a considerable number of individuals with urinary tract infections (UTIs). Another category of microorganisms, staphylococci, is Gram-positive cocci detected in the human microbiota. Staphylococcus aureus is an opportunistic pathogen, capable of causing deep, superficial, and toxigenic infections (Correa et al., 2020). Methicillin-resistant Staphylococcus aureus (MRSA) is resistant to all β-lactam antimicrobials. It infects and colonizes animals and humans, who are considered the main reservoirs of these microorganisms. MRSA-infected animal-origin foods also serve as a transmission vehicle, with prevalence in the production chain from ruminants to dairy products (Papadopoulos et al., 2018). Within the realm of significant microorganisms, there is the bacterium Klebsiella pneumoniae carbapenemase-producing (KPC), discovered in the 2000s in the United States. It has become a microorganism resistant to antibiotics and is a public health problem due to its global spread. This issue leads to hospital costs, and mortality, and presents adverse effects in its treatment, such as hepatotoxicity and nephrotoxicity. This underscores the need for studies to discover effective methods to combat it (Castañeda et al., 2018).

When it comes to fungi, the species Candida albicans is the causative agent of candidiasis. It can affect the mouth, oropharynx, vagina, gastrointestinal tract, and skin. Its occurrence can occur in both healthy individuals and those weakened by chronic diseases, antibiotic use, catheter use, neoplasms, and, as a result of the illness, a decrease in immunity (Correa et al., 2020).

3 Methodology

For the development of this bibliographic research, the search covered studies from 2014 to 2023. In Figure 3, a flowchart illustrates how the research was conducted. In the identification process, various research sites were utilized, including Portal Capes, Scopus, Science Direct, and Google Scholar. English keywords were used for article selection. Exclusion criteria involved work unrelated to biological activities or where access to the complete work was not permitted.

Eligibility and Inclusion

Article

selection

Identification Process

Portal Capes, Scopus, Science direct, google acadêmico

150 articles were consulted using the database and selected based on searches in abstracts, titles, and/or keywords

75 articles used

10 articles excluded

“green synthesis”, “gold and silver nanoparticles”, “plant extract root flower leaf stalk”, “brazilian ginseng”, “antimicrobial activity”, “Pfaffia”, “sustainability”

22 articles included in the literature review

Figure 3. Methodology flowchart. Source: Authors, 2023

4 Results and Discussion

After extensive research, several scientific articles dedicated to the studies of various types of ginseng were found, with special emphasis on the species P. ginseng. Regarding P. glomerata, it was observed that no studies were found on the use of the plant as a green synthesis of NPMs with applications in biological activity. The data regarding the parameters, time, morphology, and biological activity of silver and gold nanoparticles from green synthesis with plant extracts were summarized in Table 1.

Table 1. Green synthesis parameters for silver and gold nanoparticles using extracts from different ginseng species. Where: NPs – Nanoparticles; M/E – ratio of metal salt to plant extract; Au – Gold; Ag – Silver

| Plant Species | Part | Type of NPs |  | Synthesis Conditions |  |  | Characterization | Microorganism | Reference |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Formation Time | Temperature (0C) | S/E | Size (nm) | Morphology |  |  |
| Ginseng Siberian | Leaf and Root | Au | 24 hours to 30 days | 28 | 20 ml of solution (4 mM HAuCl4) / 1.5 mL extract | 200 | Spherical | Murine B16 melanoma cells | Fenglian et al. (2019) |
| Panax ginseng | Leaf and Root | Au and Ag | Au - 3 min Ag - 45 min | 80 | 1mL (0.1 mM HAuCl4)/1g of the powder | AuNP – 10 to 20 Ag NP – 5 to 15 | AuNP - Spherical | E.coli, S.enterica, Vibrio parahaemolyticus, S.aureus, Bacillus anthracis e Bacillus cereus | Singh; Kim; Yang (2015) |
| Panax ginseng Meyer (White Ginseng) | Raiz | Au and Ag | Ag -120min Au – 5min | 80 | 1mM of (Ag or Au) for 50mg/mL of the extract | AuNPs: 10-40 AgNPs: 10-30 |  | E. coli e S. aureus | Wang et al. (2016) |
| Panax ginseng Meyer (Red Ginseng) | Raiz | Au and Ag | Ag -60 min Au -10 min | 80 | 1mM of (Ag or Au)/50mg/mL of the extract | AuNPs: 10-30 AgNPs: 10-30 | AuNPs - Spherical AgNPs - Spherical | E. coli e S. aureus | Wang et al. (2016) |
| Panax ginseng Meyer (Black Ginseng) | Raiz | Au and Ag | Ag -60 min Au - 3 min | 90 | 1mM of (Ag or Au)/50mg/mL of the extract | AuNPs: 5-30 AgNPs: 5-30 | AuNPs - Icosahedral AgNPs - Spherical | E. coli e S. aureus | Wang et al. (2016) |
| Panax ginseng | Leaf | Ag | - | 80 | 5 mM (Ag)/0.15 g/mL of extract | - | - | A549 lung cancer cell MCF7 breast cancer cell HepG2 hepatocellular carcinoma cell | Castro-Aceituno, Verónica et al. (2016) |
| Panax ginseng | Leaf | Au | 3 min | 80 | 1mM (Au)/150mg/mL of extract | 10-20 nm |  | Human dermal fibroblast and murine B16BL6 melanoma cell lines | Jiménez-Pérez, Zuly Elizabeth et al. (2018) |
| Red Ginseng | Root | Ag and Au | – | 80 | 1mM of (Ag or Au) / 100mg/mL extract | 10–30 nm | Spherical | Vibrio parahaemolyticu, S. aureus, Bacillus cereus, Candida albicans and Pseudomonas aeruginosa. | Priyanka Singh et. al (2016) |
| Ginseng siberiano | Leaf and Stem | Au | - | - | 4 mM (Au)/1000 mg/mL of extract | 200 nm | Spherical | B16 melanoma cells |  |
| Panax ginseng | Root | Ag | 24h | 25 | 9volumes of 1 mM (Ag)/1 volume of extract, 1 g/5 mL of water | 50–90 nm | Spherical | F. graminearum, F. avenaceum, F. poae, and F. sporotrichioides | Yugay, Yulia et al. (2021) |

Fenglian et al. (2019) synthesized gold nanoparticles using Siberian Ginseng, and characterization through UV-vis, FTIR, and TEM revealed the formation of spherical particles with an average diameter of 200 nm, encapsulated by polyphenolic compounds. The anticancer properties against melanoma cells were studied, and the cytotoxicity of the obtained nanoparticles was minimal. The authors report that further studies should be conducted, particularly evaluating the effect of the presence of metallic nanoparticles in the human body

In the studies conducted by Singh et al. (2015), the authors successfully synthesized silver and gold nanoparticles using red ginseng extract without any additional agent to stabilize the nanoparticles. The obtained nanoparticles had sizes ranging from 10 to 30 nm, and they exhibited monodispersity concerning the size distribution of the materials. In this research, the obtained NMPs were considered stable after one month of synthesis, as UV-Vis spectra did not show significant changes in the bands related to the NMPs. The antimicrobial activity of AgNPs was evaluated against E. coli, S. enterica, Vibrio parahaemolyticus, S. aureus, Bacillus anthracis, and Bacillus cereus. The study also demonstrated the potential inhibition of biofilm formation against S. aureus and P. aeruginosa.

In the study conducted by Castro-Aceituno et al. (2016), the authors investigated the anticancer potential of AgNPs synthesized with Dendropanax morbifera Léveille extract, assessing the cytotoxicity of the particles. However, the study did not provide specific details regarding the synthesis and characterization of the nanomaterial. The authors examined the effect on various types of cancer cells and observed that the AgNPs reduced cell viability, inhibited cell migration, and induced cellular apoptosis. At the end of the study, the researchers suggested that the mechanism of action of the nanoparticles still needs further investigation.

Jiménez-Peres et al. (2017) investigated various properties of silver nanoparticles, such as antioxidant properties, moisture retention capacity, activity of mushroom tyrosinase, and effects on melanin cells. The authors observed that the antioxidant properties of the nanoparticles are enhanced due to the presence of ginseng extract stabilizing the particle. The nanoparticles exhibited moisturizing properties similar to the glycerin standard and also demonstrated inhibitory activity against mushroom tyrosinase. The results indicated that gold nanoparticles could be a promising multifunctional component in cosmetics.

In the research conducted by Yugay et al. (2021), 24 hours at 25 °C were required for the formation of AgNPs. After physicochemical characterization, it was determined that the obtained particles were spherical, with sizes ranging from 50 to 90 nm, and the surface was protected by compounds derived from ginseng extract, demonstrating the efficiency of this extract in reducing and stabilizing metallic nanomaterials. The AgNPs obtained exhibited antifungal effects against F. graminearum, F. avenaceum, F. poae, and F. sporotrichioides. Additionally, the nanoparticles demonstrated a fungistatic effect, inhibiting the growth of fungi on wheat grains and preventing issues in plant growth and morphology.

In the study conducted by Wang et al. (2019), an ethanolic extract of Panax notoginseng leaves was used for the synthesis of AuNPs. The obtained NPs remained stable for 30 days, with no significant changes in the UV-Vis data. The observed morphology included spherical, oval, hexagonal, and triangular shapes, with average sizes ranging from 80 to 12 nm. In the infrared spectroscopy, various bands related to compounds present in the P. notoginseng extract were observed. Antitumor and cytotoxicity tests were also performed against pancreatic cells, revealing the nanoparticles' anticancer effects.

In Singh et al.'s work (2017), although the synthesis of nanoparticles (NPs) was not the primary objective, some properties of this material were evaluated in comparison to precursor salts, revealing higher antioxidant activity by DPPH in the NPs. According to the authors, this enhancement was attributed to the presence of Panax ginseng leaf extract. The study also investigated the effect of NPs on cell viability, anticancer activity, and inhibition of nitric oxide production. The results demonstrated that AgNPs derived from ginseng exhibit important characteristics for biomedical applications. Therefore, green synthesis using ginseng extract is considered both cost-effective and advantageous for the development of herbal remedies.

In the research by Gouyau et al. (2021), citrate-coated metallic nanoparticles (NMPs) were synthesized. The study indicated that gold nanoparticles (AuNPs) showed mild bacterial activity against E. coli and S. aureus. On the other hand, silver nanoparticles (AgNPs) exhibited high antibacterial activity against E. coli, including multidrug-resistant strains.

Naik; Devi (2021) compared the antimicrobial action of Momordica dioica-based AgNPs against S. aureus, B. subtilis, E. coli, P. aeruginosa, K. planticola, and C. albicans. It was observed that there was leakage of intracellular content from the evaluated microorganisms after exposure to AgNPs, leading to microbial cell death due to membrane damage. According to the authors, this effect occurs due to the induction of oxidative stress in the pathogens, confirming their potential applicability both as therapeutic agents and in the pharmaceutical industry.

According to Sharma et al. (2015), the toxicity of nanoparticles (NPs) varies depending on their charge, chemistry, and the organic coating on their surface. The fate and toxicity of humans and the ecosystem are still not well understood. Generally, gold and silver NPs exhibit cytotoxicity and ecotoxicity against bacteria, aquatic organisms, and plants. The toxic mechanism involves the generation of reactive oxygen species (ROS) and DNA damage caused by AgNPs or released Ag+ ions, as exemplified in Drosophila melanogaster.

A study investigated the toxicity of naturally formed AgNPs, finding that the encapsulating material of the NP influences the Minimum Inhibitory Concentration (MIC) (Sharma et al., 2015). In other words, regardless of the metal employed, the encapsulating material plays a crucial role in the antimicrobial activity of the nanoparticles.

Singh et al. (2015) found that AgNPs with extracts from Panax ginseng roots exhibited antimicrobial activity against Escherichia coli, Salmonella enterica, Vibrio parahaemolyticus, Staphylococcus aureus, Bacillus anthracis, and Bacillus cereus. Both the proposed AgNPs and AuNPs demonstrated anticoagulant action. The authors considered the proposed methodology to be rapid, easy, environmentally friendly, and highly economical, with the potential for application across a wide biological spectrum and on a large scale. This suggests the possibility of future innovations in these syntheses. The AuNPs produced from Penicillium crustosum by Barabadi et al. (2014) exhibited a UV-Vis absorption band resulting from aromatic amino acids of proteins. The FTIR spectrum showed peaks at 3432 cm-1 associated with O-H stretching and at 2922.26 cm-1 attributed to the C-H stretch of methylene groups in proteins. The bands at 1407.36 and 1629.91 cm-1 corresponded to the N-H curve of primary amines and carbonyl stretching in proteins, respectively. The obtained AuNPs had an average size of 100 nm and a spherical shape after experimental optimization.

In the study by Madhumitha, Elango, and Roopan (2014), AgNPs synthesized with chemical reagents using different methods had their stability observed based on morphological characteristics. The researchers reported the effectiveness and safety of these AgNPs, proposing mechanisms for their interaction against methicillin-resistant Staphylococcus aureus (MRSA) in human cells. According to the authors, silver is a suitable metal for applications in the field of medicine and for use in living organisms. AgNPs were found to kill bacteria at low concentrations, in the range of mg/L, without acute toxicity in human cells. The use of AgNPs associated with polymers can enhance antimicrobial action. Colloidal solutions prepared with AgNPs can remain stable for up to six months, and it was observed that advanced synthetic techniques with greater dispersion stability increase antibacterial activity.

According to Viana et al. (2021), predictions suggest that by 2050, bacterial infections could lead to the deaths of ten million patients per year. These authors found that AgNPs synthesized from cashew tree extracts and curcumin exhibited inhibitory action against S. aureus, with nanoparticle sizes of 20 nm.

To assess the physical size of NPs, microscopy techniques can be employed when in their solid state. In a liquid medium, Dynamic Light Scattering (DLS) is commonly used. Fourier Transform Infrared Spectroscopy (FTIR) is a simple and cost-effective method that indicates the presence of functional groups in molecules during the bio-reduction of metal ions (SARGAZI et al., 2022).

NPs can also be successfully employed as a chromium adsorbent, contributing to the treatment of wastewater, according to Ren et al. (2017). These authors proposed the synthesis of porous magnetite NPs using titanium residue as an oxidizing agent and pyrite as a reducing agent in a controlled atmosphere. Thus, NPs can contribute to sustainable development and environmental protection, including promoting waste recycling initiatives.

5 Conclusion

Metallic silver and gold nanoparticles produced through green synthesis using extracts from ginseng species and similar plants have significant potential applications as anticancer and antibacterial agents. The majority of scientific studies have focused on P. ginseng, known as Korean ginseng, due to its medicinal properties and health benefits. Regarding microorganisms studied, E. coli and S. aureus have been the primary focus of research. In general, the formation time of AuNPs (gold nanoparticles) presents a significant advantage as they form in a considerably shorter time compared to AgNPs (silver nanoparticles).

In this context, the results of this study contribute valuable insights into the mechanisms of nanoparticle formation using plant extracts. There is a highlighted need for further research on green synthesis, aiming to explore the contributions of the studied species, particularly P. glomerata.

6 References

Abisharani, J. M., Devikala, S., Kumar, R. D., Arthanareeswari, M., & Kamaraj, P. (2019). Green synthesis of TiO2 nanoparticles using Cucurbita pepo seeds extract. Materials Today: Proceedings, 14, 302–307. https://doi.org/10.1016/j.matpr.2019.04.151

Adam, R., & Khan, S. B. (2021). Antimicrobial efficacy of silver nanoparticles against Candida albicans: A systematic review protocol. Plos One, 16(1), 1-13. https://doi.org/10.1371/journal.pone.0245811

Albarelli, J., Vardanega, R., Wilkins, N., Santos, D. T., Maréchal, F., & Meireles, M. A. A. (2016). Economical analysis of a pressurized fluid-based process applied for phytochemicals recovery in a sustainable biorefinery concept for Brazilian ginseng roots. Chemical Engineering Transactions, 50, 355-360. https://doi.org/10.3303/CET1650060

Balakumaran, M. D., Ramachandran, R., Balashanmugam, P., Mukeshkumar, D. J., & Kalaichelvan, P. T. (2015). Mycosynthesis of silver and gold nanoparticles: Optimization, characterization and antimicrobial activity against human pathogens. Microbiological Research, 182, 8-20. https://doi.org/10.1016/j.micres.2015.09.009

Balouiri, M., Sadiki, M., & Ibn Souda, S. K. (2015). Methods for in vitro evaluating antimicrobial activity: A review. Journal of Pharmaceutical Analysis, 6(2), 71-79. https://doi.org/10.1016/j.jpha.2015.11.005

Balastretri, C., Sakai, O. A., Barros, B. C. B., Seixas, F. A. V., Sato, F., Ogawa, C. Y. L., Rocha, S. A., & Mello, J. C. P. (2018). Estudo comparativo entre técnicas de extração convencional e limpa e caracterização dos biocompostos do ginseng brasileiro Pfaffia glomerata utilizando FT-RAMAN e FT-NIR. Advances in Cleaner Production, 7, 1-9.

Baláž, M., Bedlovičová, Z., Daneu, N., Siksa, P., Sokoli, L., Tkáčiková, L., Salayová, A., Džunda, R., Kováčová, M., Bureš, R., & Bujňáková, Z. L. (2021). Mechanochemistry as an alternative method of green synthesis of silver nanoparticles with antibacterial activity: A comparative study. Nanomaterials, 11(5), 1139. https://doi.org/10.3390/nano11051139

Barabadi, H., Honary, S., Ebrahimi, P., Mohammadi, M. A., Alizadeh, A., & Naghibi, F. (2014). Microbial mediated preparation, characterization, and optimization of gold nanoparticles. Brazilian Journal of Microbiology, 45(4), 1493-1501. https://doi.org/10.1590/S1517-83822014000400046

Behravan, M., Panahi, A. H., Naghizadeh, A., Ziaee, M., Mahdavi, R., & Mirzapour, A. (2018). Facile green synthesis of silver nanoparticles using Berberis vulgaris leaf and root aqueous extract and its antibacterial activity. International Journal of Biological Macromolecules, 124, 148-154. https://doi.org/10.1016/j.ijbiomac.2018.11.101

Carmona, R. E., Benito, N., Plaza, T., & Sánchez, G. R. (2017). Green synthesis of silver nanoparticles by using leaf extracts from the endemic Buddleja globosa Hope. Green Chemistry Letters and Reviews, 10(4), 250-256. https://doi.org/10.1080/17518253.2017.1360400

Castañeda, J. A. R., Ravina, A. R., Lorenzo, R. B., Gonzalez, J. E. P., Campos, J. C. S., & Salinas, D. F. (2018). Mortality due to KPC carbapenemase-producing Klebsiella pneumoniae infections: Systematic review and meta-analysis: Mortality due to KPC Klebsiella pneumoniae infections. Journal of Infection, 76(5), 438-448. https://doi.org/10.1016/j.jinf.2018.02.007

Castro-Aceituno, V., Ahn, S., Simu, S. Y., Singh, P., Mathiyalagan, R., Lee, H. A., & Yang, D. C (2016). Anticancer activity of silver nanoparticles from Panax ginseng fresh leaves in human cancer cells. Biomedicine & Pharmacotherapy, 84, 158-165. https://doi.org/10.1016/j.biopha.2016.09.016

Chen, J., Luo, H., Shi, H., Li, G., & An, T. (2014). Anatase TiO2 nanoparticles-carbon nanotubes composite: Optimization synthesis and the relationship of photocatalytic degradation activity of acyclovir in water. Applied Catalysis A: General, 485, 188-195. https://doi.org/10.1016/j.apcata.2014.08.004

Correa, L. T., Nicoletti, M. A., De Amorim, C. S., Da Costa, A. R., Leoni, L. A. B., Munõz, J. W. P., & Fukushima, A. R. (2020). Atividade antimicrobiana do óleo essencial de Melaleuca e sua incorporação em um creme mucocutâneo. Revista Fitos, v. 14, n. 1. https://doi.org/10.32712/2446-4775.2020.818

Deshmukh, A. R., Gupta, A., & Kim, B. S. (2019). Ultrasound-assisted green synthesis of silver and iron oxide nanoparticles using fenugreek seed extract and their enhanced antibacterial and antioxidant activities. BioMed Research International, 2019, 1-13. https://doi.org/10.1155/2019/1714358

Elsharkawy, E. R. (2018). Antimicrobial activity of silver nanoparticles, synthesis by green method from Artemisia monosperma. Oriental Journal of Chemistry, 34(3), 1420-1426. http://dx.doi.org/10.13005/ojc/340331

Fenglian, W., Zhu, J., Li, G., Wang, J., Veeraraghavan, V. P., Mohan, S. K., & Zhang, Q. (2019). Biologically synthesized green gold nanoparticles from Siberian ginseng induce a growth-inhibitory effect on melanoma cells (B16). Artificial Cells, Nanomedicine, and Biotechnology, 47(1), 3297-3305. https://doi.org/10.1080/21691401.2019.1647224

Gerontakos, S., Taylor, A., Avdeeva, A. Y., Shikova, V. A., Pozharitskaya, O. N., Casteleijn, D., Wardle, J., & Shikov, A. N. (2021). Findings of Russian literature on the clinical application of Eleutherococcus senticosus (Rupr. & Maxim.): A narrative review. Journal of Ethnopharmacology, 278, 114274. https://doi.org/10.1016/j.jep.2021.114274

Mohsin, M. M., Hanif, M. A., Ayub, M. A., & Dharmadasa, R. M. (2020). Ginseng. In Medicinal Plants of South Asia (pp. 331-340). Elsevier.

Gouyau, J., Duval, R. E., Boudier, A., & Lamouroux, E. (2021). Investigation of nanoparticles metallic core antibacterial activity: Gold and silver nanoparticles against Escherichia coli and Staphylococcus aureus. International Journal of Molecular Sciences, 22(1905). https://doi.org/10.3390/ijms22041905.

Hakimi, F., Rashchi, F., Dolati, A., & Astaraei, F. R. (2019). Anodizing Pb electrode for synthesis of β-PbO2 nanoparticles: Optimization of electrochemical parameters. Journal of the Electrochemical Society, 166(13), 617-625. https://doi.org/10.1149/2.0551913jes

Hanif, M. A. (2019). Muhammad Mubeen Mohsin, Muhammad Asif Hanif, Muhammad Adnan Ayub 2, Ijaz Ahmad Bhatti, Muhammad Idrees Jilani 3. Medicinal Plants of South Asia, 231.

Hulkoti, N. I., & Taranath, T. C. (2014). Biosynthesis of nanoparticles using microbes – A review. Colloids and Surfaces B: Biointerfaces, 121, 474-483. https://doi.org/10.1016/j.colsurfb.2014.05.027

Huang, R., Cui, X., Luo, X., Mao, P., Zhuang, P., Li, Y., Li, Y., & Li, Z. (2021). Effects of plant growth regulator and chelating agent on the phytoextraction of heavy metal by Pfaffia glomerata and on the soil microbial community. Environmental Pollution, 283, 1-14. https://doi.org/10.1016/j.envpol.2021.117159

Ishak, N. A. I., Kamarudin, S. K., & Timmiati, S. N. (2019). Green synthesis of metal and metal oxide nanoparticles via plant extracts: an overview. Material Research Express, 6, 11. https://doi.org/10.1088/2053-1591/ab4458

JankauskaitĿ, V., VitkauskienĿ, A., Lazauskas, A., Baltrusaitis, J., ProsyĿevas, I., & AndruleviĿius, M. (2016). Bactericidal effect of graphene oxide/Cu/Ag nano derivatives against Escherichia coli, Pseudomonas aeruginosa, Klebsiella pneumoniae, Staphylococcus aureus, and Methicillin-resistant Staphylococcus aureus. International Journal of Pharmaceutics, 511(1), 90-97. https://doi.org/10.1016/j.ijpharm.2016.06.121

Jiménez-Pérez, Z. E., Singh, P., Kin, Y. J., Mathiyalagan, R., Kim, D. Y., Lee, M. H., & Yang, D. C. (2017). Applications of Panax ginseng leaves mediated gold nanoparticles in cosmetics: Relation to antioxidant, moisture retention, and whitening effect on B16BL6 cells. Journal of Ginseng Research. https://doi.org/10.1016/j.jgr.2017.04.003

Kalita, D., & Baruah, S. (2019). The impact of nanotechnology on food. In R. do Nascimento, O. P. Ferreira, A. J. de Paula, & V. D. O. S. Neto (Eds.), Nanomaterials Applications for Environmental Matrices (pp. 369–379). Elsevier: Amsterdam, The Netherlands.

Khan, M. A., Wu, V. M., Ghosh, S., & Uskokovic, V. (2016). Gene delivery using calcium phosphate nanoparticles: Optimization of the transfection process and the effects of citrate and poly(L-lysine) as additives. Journal of Colloid and Interface Science, 471, 48-58. https://doi.org/10.1016/j.jcis.2016.03.007

Kuppusamy, P., Yusoff, M. M., Maniam, G. P., & Govindan, N. (2014). Biosynthesis of metallic nanoparticles using plant derivatives and their new avenues in pharmacological applications – An updated report. Saudi Pharmaceutical Journal, 24(4), 473-484. https://doi.org/10.1016/j.jsps.2014.11.013

Leal, C., Gouvinhas, I., Santos, R. A., Rosa, E., Silva, A. M., Saavedra, M. J., & Barros, A. I. R. N. A. (2020). Potential application of grape (Vitis vinifera L.) stem extracts in the cosmetic and pharmaceutical industries: Valorization of a by-product. Industrial Crops & Products, 154, 1-11. https://doi.org/10.1016/j.indcrop.2020.112675

Li, W. H., & Yang, N. (2016). Green and facile synthesis of Ag-Fe3O4 nanocomposites using the aqueous extract of Crataegus pinnatifida leaves and their antibacterial performance. Materials Letters, 162, 157-160. https://doi.org/10.1016/j.matlet.2015.09.064

Madhumitha, G., Elango, G., & Roopan, S. M. (2014). Bio-functionalized doped silver nanoparticles and their antimicrobial studies. Journal of Sol-Gel Science and Technology, 98, 5289–5300. https://doi.org/10.1007/s10971-014-3591-2

Manandhar, S., Luitel, S., & Dahal, R. K. (2019). In vitro antimicrobial activity of some medicinal plants against human pathogenic bacteria. Journal of Tropical Medicine, 2019, 1-6. https://doi.org/10.1155/2019/1895340

Martins, N. M. (2020). Pfaffia glomerata (Spreng.) Pedersen: Estudo em extrato aquoso e síntese verde de nanopartículas de ouro. Dissertação (Mestrado em Sustentabilidade) – IFPR/UEM, Umuarama, p. 40.

Maurya, A., Prasad, J., Das, S., & Dwivedy, A. K. (2021). Essential oils and their application in food safety. Frontiers in Sustainable Food Systems, 5. https://doi.org/10.3389/fsufs.2021.653420

Naik, S., & Devi, C. V. R. (2021). Phyto-fabricated silver nanoparticles inducing microbial cell death via reactive oxygen species-mediated membrane damage. IET Nanobiotechnology, 15, 492-504. https://doi.org/10.1049/nbt2.12036

Neves, C. S., Gomes, S. S. I., Santos, T. R., Almeida, M. M., Souza, Y. O., Garcia, R. M. G., Otoni, W. C., Chedier, L. M., Raposo, N. R. B., Viccini, L. F., & Campos, J. M. S. (2016). “Brazilian ginseng” (Pfaffia glomerata Spreng. Pedersen, Amaranthaceae) methanolic extract: Cytogenotoxicity in animal and plant assays. South African Journal of Botany, 106, 174-180. https://doi.org/10.1016/j.sajb.2016.07.003

Oliveira, C. B. D. (2018). Caracterização química do extrato do Ginseng-brasileiro (Pfaffia glomerata (Spreng.) Pedersen) Obtido por extração supercrítica via líquido pressurizado (PLE) e por soxhlet. Dissertação (Mestrado em Sustentabilidade) – IFPR/UEM, Umuarama, p. 18-23.

Oliveira, U., Paglia, A. P., Brescovit, A. D., Carvalho, C. J. B., Silva, D. P., Rezende, D. T., Leite, F. S. F., Batista, J. A. N., Barbosa, J. P. P. P., Stehmann, J. R., Ascher, J. S., Vasconcelos, M. F., Junior, P. M., Neto, P. L., Dias, P. G., Ferro, V. G., Santos, A. J. (2016). The strong influence of collection bias on biodiversity knowledge shortfalls of Brazilian terrestrial biodiversity. Diversity and Distributions, 1-13. https://doi.org/10.1111/ddi.12489

Papadopoulos, P., Papadopoulos, T., Angelidis, A. S., Boukouvala, E., Zdragas, A., Papa, A., Hadjichristodoulou, C., & Sergelidis, D. (2018). Prevalence of Staphylococcus aureus and methicillin-resistant S. aureus (MRSA) along the production chain of dairy products in north-western Greece. Food Microbiology, 69, 43-50. https://doi.org/10.1016/j.fm.2017.07.016

Porto, K. B. (2012). Ação antimicrobiana das nanopartículas de prata sobre patógenos. Monografia (Graduação em Odontologia) – USF, Bragança Paulista, 29.

Singh, P., Kim, Y. J., Wang, C., Mathiyalagan, R., & Yang, D. C. (2016). The development of a green approach for the biosynthesis of silver and gold nanoparticles by using Panax ginseng root extract, and their biological applications. Artificial Cells, Nanomedicine, and Biotechnology, 44(4), 1150-1157. https://doi.org/10.3109/21691401.2015.1011809

Qasim, M., Singh, B. R., Naqvi, A. H., Paik, P., & Das, D. (2015). Silver nanoparticles embedded mesoporous SiO2 nanosphere: an effective anticandidal agent against Candida albicans 077. Nanotechnology, 26(28). https://doi.org/10.1088/0957-4484/26/28/285102

Rai, M. (2013). Nanobiotecnologia verde: biossínteses de nanopartículas metálicas e suas aplicações como nanoantimicrobianos. Ciência & Cultura, 65(3), 44-48.

Rajan, P. I., Vijaya, J., Jesudoss, S. K., Kaviyarasu, K., Lee, S. C., Kennedy, L. J., Jothiramalingam, R., Lohedan, H. A. A., & Abdullah, M. (2018). Investigation on preferably oriented abnormal growth of CdSe nanorods along (0002) plane synthesized by henna leaf extract-mediated green synthesis. Royal Society Open Science, 5(3), 171430. https://doi.org/10.1098/rsos.171430

Ren, G., Wang, X., Huang, P., Zhong, B., Zhang, Z., Yang, L., & Yang, X. (2017). Chromium (VI) adsorption from wastewater using porous magnetite nanoparticles prepared from titanium residue by a novel solid-phase reduction method. Science of the Total Environment, 607-608, 900-910. https://doi.org/10.1016/j.scitotenv.2017.06.103

Ribeiro, A. S., Estanqueiro, M., Oliveira, M. B., & Lobo, J. M. S. (2015). Main benefits and applicability of plant extracts in skin care products. Cosmetics, 2(2), 48-65. https://doi.org/10.3390/cosmetics2020048

Saravanan, A., Kumar, P. S., Karishma, S., Vo, D. V. N., Jeevanantham, S., Yaashikaa, P. R., & George, C. S. (2021). A review on biosynthesis of metal nanoparticles and its environmental applications. Chemosphere, 264, 128580. https://doi.org/10.1016/j.chemosphere.2020.128580

Sargazi, S., Laraib, U., Er, S., Rahdar, A., Hassanisaadi, M., Zafar, M. N., Pascual, A. M. D., & Bilal, M. (2022). Application of green gold nanoparticles in cancer therapy and diagnosis. Nanomaterials, 12(1102). https://doi.org/10.3390/nano12071102

Sathishkumar, P., Preethi, J., Vijayan, R., Yusoff, A. R. M., Ameen, F., Suresh, S., ... & Palvannan, T. (2016). Anti-acne, anti-dandruff, and anti-breast cancer efficacy of green synthesized silver nanoparticles using Coriandrum sativum leaf extract. Journal of Photochemistry and Photobiology B: Biology, 163, 69-76. https://doi.org/10.1016/j.jphotobiol.2016.08.005

Sharma, V. K., Filip, J., Zboril, R., & Varma, R. S. (2015). Natural inorganic nanoparticles–formation, fate, and toxicity in the environment. Chemical Society Reviews, 44(23), 8410-8423. https://doi.org/10.1039/C5CS00236B

Sheldon, R. A. (2017). The E factor 25 years on the rise of green chemistry and sustainability. Green Chemistry, 19(1), 18-43.

Siakavella, I. K., Lamari, F., Papoulis, D., Orkoula, M., Gkolfi, P., Lykouras, M., Avgoustakis, K., & Hatziantoniou, S. (2020). Effect of plant extracts on the characteristics of silver nanoparticles for topical application. Pharmaceutics, 12(1244). https://doi.org/10.3390/pharmaceutics12121244

Silva, L. P., Bonatto, C. C., Pereira, F. D. E. S., Silva, L. D., Albernaz, V. L., & Polez, V. L. P. (2017). Nanotecnologia verde para síntese de nanopartículas metálicas. In Biotecnologia Aplicada à Agro & Indústria - v. 4 (pp. 967-1012). São Paulo: Blucher.  https://doi.org/10.5151/9788521211150-26.

Silva, T. D., Chagas, K., Batista, D. S., Felipe, S. H. S., Louback, E., Machado, L. T., Fernandes, A. M., Buttrós, V. H. T., Koehler, A. D., Farias, L. M., Santos, A. F., Silva, P. O., Otoni, W. C. (2019). Morphophysiological in vitro performance of Brazilian ginseng (Pfaffia glomerata (Spreng.) Pedersen) based on culture medium formulations. In Vitro Cellular & Developmental Biology – Plant, 55, 454-467. https://doi.org/10.1007/s11627-019-10003-9

Singh, P., Kim, Y. J., & Yang, D. C. A. (2015). Strategic approach for rapid synthesis of gold and silver nanoparticles by Panax ginseng leaves. Artificial Cells Nanomedicine, and Biotechnology, 44(8), 1949-1957. https://doi.org/10.3109/21691401.2015.1115410

Singh, P., Kim, Y. J., Wang, C., Mathiyalagan, R., & Yang, D. C. (2015). The development of a green approach for the biosynthesis of silver and gold nanoparticles by using Panax ginseng root extract, and their biological applications. Artificial Cells Nanomedicine, and Biotechnology, 44(4), 1150-1157. https://doi.org/10.3109/21691401.2015.1011809

Singh, P., Singh, H., Ahn, S., Castro-Aceituno, V., Jiménez, Z., Simu, S. Y., Kim, Y. J., & Yang, D. C. (2017). Pharmacological importance, characterization, and applications of gold and silver nanoparticles synthesized by Panax ginseng fresh leaves. Artificial Cells, Nanomedicine, and Biotechnology, 45(7), 1415–1424. https://doi.org/10.1080/21691401.2016.1243547

Srikar, S. K., Giri, D. D., Pal, D. B., Mishra, P. K., & Upadhyay, S. N. (2016). Green synthesis of silver nanoparticles: a review. Green and Sustainable Chemistry, 6(1), 34-56.  https://doi.org/10.4236/gsc.2016.61004

Vardanega, R., Santos, D. T., & Meireles, M. A. A. (2016). Proposal for fractionating Brazilian ginseng extracts: Process intensification approach. Journal of Food Engineering, 196, 73-80. https://doi.org/10.1016/j.jfoodeng.2016.10.018

Viana, A. V., Viana, D. S. F., Figueirêdo, G. S., Brito, J. E., Viana, V. G. F., & Junior, V. G. F. V. (2021). Potencial antimicrobiano das nanopartículas de prata estabilizadas em curcumina e extrato de folhas de cajueiro (Anacardium occidentale L.). Research, Society and Development, 10(9). http://dx.doi.org/10.33448/rsd-v10i9.18364

Wang, D., Markus, J., Kim, Y., Wang, C., Pérez, Z. E. J., Ahn, S., ... Yang, D. C. (2016). Coalescence of functional gold and monodisperse silver nanoparticles mediated by black Panax ginseng Meyer root extract. International Journal of Nanomedicine, 11, 6621-6634. https://doi.org/10.2147/IJN.S113692

Wang, L., Huang, Y., Yin, G., Wang, J., Wang, P., Chen, Z. Y., Wang, T., & Ren, G. (2020). Antimicrobial activities of Asian ginseng, American ginseng, and notoginseng. Phytotherapy Research, 34(6), 1226-1236. https://doi.org/10.1002/ptr.6605

Wang, L., Xu, J., Yan, Y., Liu, H., & Li, F. (2019). Synthesis of gold nanoparticles from leaf Panax notoginseng and its anticancer activity in pancreatic cancer PANC-1 cell lines. Artificial Cells, Nanomedicine, and Biotechnology, 47(1), 1216–1223. https://doi.org/10.1080/21691401.2019.1593852

Wongyai, K., Wintachai, P., Maungchang, R., & Rattanakit, P. (2020). Exploration of the antimicrobial and catalytic properties of gold nanoparticles greenly synthesized by Cryptolepis buchanani Roem. and Schult extract. Journal of Nanomaterials, 1320274. https://doi.org/10.1155/2020/1320274

Yaqoob, A. A., Umar, K., & Ibrahim, M. N. M. (2020). Silver nanoparticles: various methods of synthesis, size affecting factors and their potential applications–a review. Applied Nanoscience, 10, 1369-1378. https://doi.org/10.1007/s13204-020-01318-w

- Yugay, Y., Rusapetova, T., Mashtalyar, D., Grigorchuk, V., Vasyutkina, E., Kudinova, O., ... & Shkryl, Y (2021). Biomimetic synthesis of functional silver nanoparticles using hairy roots of Panax ginseng for wheat pathogenic fungi treatment. Colloids and Surfaces B: Biointerfaces, 207, 112031. https://doi.org/10.1016/j.colsurfb.2021