Comment [D.P1]: Change title

Comment [D.P2]: grammar

Comment [D.P4]: Brief introduction is requir

Comment [D.P6]: Specify the objectives

Comment [D.P7]: Specify the values and poin out conclusion and significance

Comment [D.P12]: spelling?

Comment [D.P13]: Not clear

Comment [D.P15]: Include these words

Comment [D.P16]: spelling

Comment [D.P17]: what does it mean, expa and explain

Comment [D.P18]: Write the objective in sentence form

Comment [D.P19]: Write a short note sweet potato and its advantages at the beginning

Comment [D.P20]: Details not complete

Comment [D.P21]: Details are required. Wh it is purchased, how much, physical appearance e

Comment [D.P22]: Name of machine?

Comment [D.P14]: Grammar

Comment [D.P11]: not clear; what is this?

Comment [D.P10]: grammar

Comment [D.P9]: Include the above sentenc highlighted in red

Comment [D.P8]: Change the order as indica below in red

Comment [D.P5]: Give details of the method

Comment [D.P3]: Use the title given below (i red)

Original research article

# Effects of Various Treatments on Sweet Potato Starch: An FTIR Study of a Natural

Biopolymer

Please use the following title

# FTIR spectrum of Starch from Sweet Potato and the Effects of Acid Treatment and Extrusion

Abstract— Sweet potato Starch from Sweet potato was extracted. and subjected to acid treatment and physical treatment (extrusion). The treated starch, acid treated starch (ATS) and physical treated starch (PMS) where analysed with the Fourier Transform Infrared Spectroscopy (FTIR). FTIR spectra obtained for the treated starches observed changes as compared to the native starch The PMS showed reduced transmittance, while the ATS showed alternating increase and decrease transmittance.

Keywords: Starch; Treatment; FTIR; Sweet potato

Sweet potato; Starch; Acid treatment; Extrusion, FTIR Spectra.

## Introduction

Starch is a polysaccharide composed of D-glucose units linked by α-glycosidic bonds.

Starch is an intricate polymer substance that consists of loose amorphous sections intermingled with ordered crystalline sections,  resulting from hydrogen bonds being formed amongst the starch molecules. Starch occurs as a scentless insoluble powder in cold water after extraction. This powder referred to as native starch consists of amylopectin and amylose parts. The amylose content ranges between 18 and 28%. while the amylopectin content ranges between 72 and 82%, Other trace elements are , minerals,  enzymes, lipids, phosphorous, proteins, nucleic acids , and amino acids. Native starches comprise of 15% to 45% of crystalline material [1]. With respect to X-ray diffraction pattern, starches are grouped into three crystalline types denoted as A, B and C. Cereal starches are of the A-type, amylose-rich cereal and tuber starches are of the B-type, whilst the C-type is typical of leguminous starches and is a mixture of A and B crystalline types. The V-type is experiential when there is formation of  complexes between a complexing molecule such as iodine and alcohols and amylose.

Native starch exhibits some downsides that limit its functional use, such as sensitivity to shearing, insolubility in cold water and low pH [2]. The main aim of native starch modification is the improvement of functional properties by altering its physico- chemical characteristics. Modification is essential for the continual and increased use of starch to provide binding, gelling, thickening, film forming and adhesiveness. The physical and/or chemical modification of starch may, therefore, enhance its applications range. Several techniques of starch modification exists with variety of characteristics and applications [3-23]. These techniques modify the starch polymer, altering its structural features and physicochemical properties thereby increasing its values for non-food and food industries[16]. Therefore, there is great interest in techniquess to alter the structure in the crystalline region, or reduce the size of crystalline regions [7]. Most methods of decreasing the regularity starch crystalline regions include chemical processes, such as acidolysis, oxidation [18], enzymatic degradation processes [21.22] and physical processes, such as heat- moisture treatment [10], radioactive degradation [24, 9], microwave degradation [6], ultrasonic degradation and extrusive degradation processes. Acid modification of starch is the treatment of starch to acids under controlled conditions. Treatment of starch with acids at any concentration, results in hydrolysis of the starch which reduces the granule size and paste viscosity [25, 26]. It is carried out using hydrochloric or sulfuric acid and the concentration of the acid affects the degree of hydrolysis. During acid hydrolysis, the amylopectin is depolymerised and this increases the quantity of linear chains similar to amylose, favouring its strength and gel formation [27]., The molecular mass of the starch grannules decreases after acid hydrolysis.	 The physical treatment viz. extrusion is defined as a process of subjecting starch in a low moisture environment to mechanical

solubulity,

shearing forces in short amounts a period of time and at high temperature[28, 29]. Extrusion improves water	reduces

the size of the starch grannules and increases the Tgel of starch, changing the molecular extension and its links, thereby increasing its amorphous nature by reducing the crystallinity of the starch [30, 31].

This work studies the effect of extrusion and acid treatments on sweet potato starch with the aid of the FTIR spectroscopy.

- MATERIALS AND METHODS

## Extraction of Starch from tubers

o

Locally sourced sweet potato tubers were washed and cleaned to remove flaws and dirts. The tubers were cut into small parts and blended with the aid of a laboratory standard blender. A 75mm-mesh sieve was used to sieve the mixture and the residue was rinsed and set aside. The filtrate was left to stand overnight at 15 C, the supernatant was cast-off while the precipitate was

reserved. The precipitate was re-suspended in distilled water and allowed to sediment repeatedly to obtain white starch. The starch was dried at 50oC for 6 hours after which the starch was ground and sieved through an 80-mesh sieve.

## Modification of Starch

Comment [D.P24]: Complete details are required; how much was taken for experiment?

Comment [D.P23]: Reference?

Physical Treatment of Starch	 The extracted sweet potato starch was modified physically by extrusion. The extracted sweet potato starch was processed by an extruder which combines several unit operations, including shaping, shearing, kneading, mixing, heating, cooling, and forming. The temperature in the extruder was set at 150°C and the residence time was 60 seconds.

## Acid Treatment of Starch

Comment [D.P25]: Reference?

100 g of dried potato starch was immersed in a beaker containing 150 ml of 6% (w/v) HCl at 40 °C, this was done in sets over 48 h with periodic stirring. A uniform dispersion of starch was obtained by careful addition of acid. After hydrolysis, the suspension was neutralized with 2% (w/v) NaOH solution and washed with distilled water thrice. The water was then extracted by centrifugation at 3000 rpm for 10 min and decantation. The wet acid-modified starch was dried at 40 °C. The dried powder was pulverised and sieved through mesh sieve of 100 micrometer to obtain acid-modified starch powder.

## Fourier Infrared Spectroscopy (FTIR).

Comment [D.P26]: Experimental details required; how much sample was taken?

Fourier transform infrared (FTIR) spectra (KBr) were recorded using a Nicolet Magna-IR 560 FTIR spectrophotometer at a frequency of 4000 to 400 cm-1.

- Results and Discussion

Comment [D.P27]: What is the objective?

Sweet potato starch was extracted and modified via extrusion and acid steeping to obtain physically modified starch and acid modified starch, respectively. The starch samples were characterized using FTIR spectroscopy to ascertain the functional groups present after modification.

## FTIR Characterization of Starch Samples

The unmodified and modified starches were characterised with the Fourier Transform Infrared Spectroscopy (FTIR) and the spectra for each starch sample is presented in Figures 1 to 3.

Comment [D.P28]: Sentence not clear

Figure 1 presents the FTIR spectra for unmodified starch and acid treated starch. Initially, the FTIR spectra of the unmodified starch presented complex vibrational modes as a result of the pyranose ring of the glycosidic units below 800 cm-1 which represents what other researchers obtained in their works [12, 15, 18]. At the 1000–1200 cm-1 region, the common features of polysaccharides were observed. This region was controlled by ring vibrations overlayed by stretching vibrations of C–OH side groups and the C–O–C glycosidic bond vibration. Within this wavenumber range, the C–C and C–O stretching vibrations results in the modes associated to the bands at 994, 1084, and 1163 cm-1 and the C–O–C glycosidic band at 860 cm-1. At 1465, 1425, and 1366 cm-1, the spectrum displays C–H bending bands. The starch spectrum demonstrated characteristic O–H stretching and bending bands at 1649 and 3430 cm-1, accredited to the complex vibrational stretches related with free, intra - and inter - molecular bound hydroxyl groups that make up the structure of starch as well as intramolecular hydrogen bond typical of polysaccharides. Peak were observed at 2929 cm-1 was meant for C-H stretches linked with the ring hydrogen atoms.

## Effect of Acid Treatment on Native Starch

Comment [D.P30]: Use correct unit

Comment [D.P29]: Reference?

For the acid treated starch spectra, slight shifts in the peaks were observed and reductions in the peaks intensity as presented in Table 1, and narrowing of the O–H broad band at 3430 cm-1. Most authors have used infrared spectroscopy to approximate the amount of crystalline regions by studying the bands at 1047 and 1022 cm-1. Thus, the crystalline state can be acknowledged by the band at 1047 cm-1, and the starch amorphous region characterized by an absorption band around 1022 cm-1[1, 2, 8, 19]. From the acid treated starch spectra it is observed that the band at 1022cm became narrower indicating disappearance of the amorphous  region of the starch which is characteristic with acid hydrolysis of starch.

## Effect of Extrusion on Native Starch

The FTIR spectrum for the physically modified starch is presented in Fig 2. From the spectra, it is evident that there are reductions in the intensity of the peaks and slight shifts in the peaks, as presented in Table 1, as well as broadening of the O–H band at 3430 cm-1. At the 1022cm-1 wavelength, which represents the starch amorphous region, a broader band is observed showing increased amorphous region of the starch which could be because of the shearing force the starch granules passed through during extrusion.

Comment [D.P35]: Include the unit

Comment [D.P34]: Include the unit

Comment [D.P33]: Include the unit

Comment [D.P32]: Use any one word throughout: native starch or unmodified starch o natural starch

Comment [D.P31]: Not clear; modify as highlighted in red below

Table 1 Peaks and bonds observed at the absorption bands in the FTIR spectra of the starch samples	 The absorption bands of various starch samples observed in the FTIR spectra

|  |  | Unmodified | Starch |  | Acid Treated |  |  | Physically Modified |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | Starch |  |  | Starch |  |  |
| O-H | 3430 |  |  |  | 3422 |  |  | 3434 |  |  |  |
| C-H | 2929 |  |  |  | 2936 |  |  | 2930 |  |  |  |
| O-H | 1649 |  |  |  | 1656 |  |  | 1647 |  |  |  |
| C-Hs | 1465 |  |  |  | 1465 |  |  | 1455 |  |  |  |
| C-H, COO | 1425 |  |  |  | 1424 |  |  | 1426 |  |  |  |
| C-O, O-H | 1163 |  |  |  | 1160 |  |  | 1161 |  |  |  |
| C-O | 1084 |  |  |  | 1080 |  |  | 1085 |  |  |  |
| C-C | 994 |  |  |  | 989 |  |  | 984 |  |  |  |
| C-O-C | 860 |  |  |  | 862 |  |  | 863 |  |  |  |

40

35

30

25

20	2936

15

3422

10

5

2929

1649

(2)

(1)

0

3430

-5

4000	3500	3000	2500	2000	1500	1000	500	0

Comment [D.P36]:

Wave number (cm-1)

Figure 1: FTIR spectra of natural starch (1), and acid treated starch (2)

40

35

30

Transmittance(%)

25

20	2929

1649

15

3430

10

5

0

3434	2935

-5

1647

(1)

(2)

4000	3500	3000	2500	2000	1500	1000	500	0

Wave number (cm-1)

Comment [D.P37]: Keep the natural starch ( below and Starch (2) above in the diagram.

Compare with the previous diagram above in Fig 1 and make consistency

Figure 2; FTIR spectra of natural starch (1), and physical modified starch (2)

Comment [D.P38]: Finger print region is upt

~1500cm-1

Comment [D.P39]: Modifiy the sentence

Comment [D.P40]: Superscript; change accordingly throughout manuscript

Comment [D.P41]: What do you want to communicate from this study?

Various treatments of starches are beneficial? Practically, economically?

Comment [D.P42]: Space? Check throughout the manuscript

Comment [D.P43]: Space?

Conclusion

The Nnative starch (NS), physically modified starch (PMS) and the Aacid treated starch (ATS) showed spectra that were similar below 800 cm-1 (Figures 1 to 2), which represents the starch fingerprint region. This region displayed the complex vibration  mode owing to the skeletal mode vibration of glucose pyranose ring [23, 32]. PMS showed an obvious change of the transmittance unlike the ATS which had same transmittance with the native starch. Moreover, PMS and ATS gave similar peaks at approximately 1161, corresponding to C-O, O-H structures. These results indicateds that after modification, the backbone  glucose units of starch were not altered. The peak at 1649 cm-1 of ATS was shifted to a higher wave number (1656 cm-1 ). This was ascribed to the water lost in the starch amorphous region[13,14], leading to an increased crystallinity of ATS after treatment. Also, a shift of the peaks of C-H and O-H stretching of ATS (2929 and 3393 cm-1 , respectively) indicates that change of structure and hydrogen bonding in ATS occurred after the modification process.

Data Availability: All data that supports the findings of this study are included in this article.

## References

- Lopez-Rubio, A., Flanagan, B. M., Gilbert ,E. P. and Gidley, M. J. (2008) A Novel Approach for Calculating Starch Crystallinity and Its Correlation with  Double Helix Content: A Combined XRD and NMR Study Biopolymers ,89, 9; 761-768 Wiley InterScience https://doi.org/10.1002/bip.21005

- Bashir K. and Aggarwal M. (2019) Physicochemical, structural and functional properties of native and irradiated starch: a review. J Food Sci Technol.; 56(2):513-523. DOI: 10.1007/s13197-018-3530-2. https://doi.org/10.1007/s13197-018-3530-2

- Kaur, L., Dhull, S. B., Kumar, P., & Singh, A. (2020). Banana starch: Properties, description, and modified variations-A review. International Journal of Biological Macromolecules, 165(Part B), 2096-2102 https://doi.org/10.1016/j.ijbiomac.2020.10.058

- Wani IA, Jabeen M, Geelani H, Masoodi FA, Saba I, Muzaffar S. (2014) Effect of gamma irradiation on physicochemical properties of Indian Horse Chestnut (Aesculus indica) starch. Food Hydrocolloids. ;35:253–263. https://dx.doi.org/10.1016/j.foodhyd.2013.06.002

- Bemiller J. N. and Huber K. C. (2015) “Physical modification of food starch functionalities,” Annual Review of Food Science and Technology, vol. 6, no. 1,

pp. 19–69. https://doi.org/10.1146/annurev-food-022814-015552

- Lewicka K., Siemion P., and Kurcok P. (2015) “Chemical modifications of starch: microwave effect,” International Journal of Polymer Science, vol. 867697. https://doi.org/10.1155/2015/867697

- Alcazar-Alay S. C. and Meireles M. A. A.(2015) “Physicochemical properties, modifications and applications of starches from different botanical  sources,” Journal of Food Science and Technology, vol. 35, no. 2, pp. 215–236, . https://doi.org/10.1590/1678-457X.6749

- Chen Y. F., Kaur L., and Singh J.(2018) Chemical modification of starch, Elsevier Ltd. https://doi.org/10.1016/B978-0-08-100868-3.00007-X

- Verma R, Jan S, Rani S, Jan K, Swer TL, Prakash KS, et al. 2018 Physicochemical and functional properties of gamma irradiated buckwheat and potato starch. Radiat Phys Chem. ;144:37–42. https://doi.org/10.1016/J.RADPHYSCHEM.2017.11.009

- Zheng B., Wang H., Shang W. et al.. (2018) “Understanding the digestibility and nutritional functions of rice starch subjected to heat-moisture treatment,” Journal of Functional Foods, vol. 45, pp. 165–172. https://doi.org/10.1016/j.jff.2018.03.041

- Barbosa J. V., Martins J., Carvalho L., Bastos M. M. S. M., and Magalhães F. D.(2019) “Effect of peroxide oxidation on the expansion of potato starch foam,” Industrial Crops and Products, vol. 137, pp. 428–435, 2019. https://doi.org/10.1016/j.indcrop.2019.05.045

- Lee Y. K. and Chang Y. H. (2019) “Structural and in vitro digestibility properties of esterified maca starch with citric acid and its application as an oil-in- water (O/W) pickering emulsion stabilizer,” International Journal of Biological Macromolecules, vol. 134, pp. 798–806. https://doi.org/10.1016/j.ijbiomac.2019.05.081

- Dang X., Chen H., Shan Z., Zhen W., and Yang M. (2019) “The oxidation of potato starch by electro-Fenton system in the presence of Fe(II) ions,” International Journal of Biological Macromolecules, vol. 121, pp. 113–119. https://doi.org/10.1016/j.ijbiomac.2018.10.012

- La Fuente C. I. A., de Souza A. T., Tadini C. C., and Augusto P. E. D. (2019) “Ozonation of cassava starch to produce biodegradable films,” International Journal of Biological Macromolecules, vol. 141, pp. 713–720, 2019. https://doi.org/10.1016/j.ijbiomac.2019.09.028

- Borah P. K., Rappolt M., Duary R. K., and Sarkar A.(2019) “Structurally induced modulation of in vitro digestibility of amylopectin corn starch upon esterification with folic acid,” International Journal of Biological Macromolecules, vol. 129, pp. 361–369, 2019. https://doi.org/10.1016/j.ijbiomac.2019.02.051

- Liu Y., Liu J., Kong J. et al. (2020) “Citrate esterification of debranched waxy maize starch: structural, physicochemical and amylolysis properties,” Food Hydrocolloids, vol. 104, article 105704, 2020. https://doi.org/10.1016/j.foodhyd.2020.105704

- Lima D. C., Villar J., Castanha N., Maniglia B. C., Matta Junior M. D., and Duarte Augusto P. E. (2020) “Ozone modification of arracacha starch: effect on structure and functional properties,” Food Hydrocoll, vol. 108, 2020. https://doi.org/10.13140/RG.2.2.10489.62565

- Liu P., Fang Y., Zhang X. et al. (2020) “Effects of multienzyme treatment on the physicochemical properties of maize starch-lauric acid complex,” Food Hydrocolloids, vol. 107, article 105941. https://doi.org/10.1016/j.foodhyd.2020.105941

- Wu C., Sun R., Zhang Q., and Zhong G. (2020) “Synthesis and characterization of citric acid esterified canna starch (RS4) by semi-dry method using vacuum-microwave-infrared assistance,” Carbohydrate Polymers, vol. 250, article 116985. https://doi.org/10.1016/j.carbpol.2020.116985

- Majzoobi M. and Farahnaky A .(2021) “Granular cold-water swelling starch; properties, preparation and applications, a review,” Food Hydrocolloids, vol. 111, article 106393, 2021. https://doi.org/10.1016/j.foodhyd.2020.106393

- Li H., Gui Y., Li J., Zhu Y., Cui B., and Guo L.(2020) “Modification of rice starch using a combination of autoclaving and triple enzyme treatment: structural, physicochemical and digestibility properties,” International Journal of Biological Macromolecules, vol. 144, pp. 500–508. https://doi.org/10.1016/j.ijbiomac.2019.12.112

- Maniglia B. C., Castanha N., Le-Bail P., Le-ail A., and Augusto P. E. D. (2021) “Starch modification through environmentally friendly alternatives: a review,” Critical Reviews in Food Science and Nutrition, vol. 61, no. 15, pp. 2482–2505. https://doi.org/10.1080/10408398.2020.1778633

- Pankaj B, Vipin K, Richa G, Somesh K S, Shikha K, Shivani S, Alankar S and Mulugeta T (2022) Structural Modifications and Strategies for Native Starch for Applications in Advanced Drug Delivery", BioMed Research International, 2188940, 14. https://doi.org/10.1155/2022/2188940

- Sofi BA, Wani IA, Masoodi FA, Saba I, Muzaffar S. Effect of gamma irradiation on physicochemical properties of broad bean starch. LWT Food Sci Technol. 2013;54:63–72. https://doi.org/10.1016/j.lwt.2013.05.021

- Hoover R. 2000 Acid Treated Starches. Food Reviews International, 16:3, 369-392, https://doi.org/10.1081/FRI-100100292

- Shujun Wang and Les Copeland(2015) Effect of Acid Hydrolysis on Starch Structure and Functionality: A Review, Critical Reviews in Food Science and Nutrition, 55:8, 1081-1097, DOI: 10:1080/10408398.2012.684551 https://doi.org/10.1080/10408398.2012.684551

- Huan Li, Rongrong Wang, Jie Liu, Qun Zhang, Gaoyang Li, Yang Shan, Shengua Ding 2020 Effects of Heat Moisture and Acid Treaments on the Structural, Physicochemical and In-vitro Digestibility porperties of Lily Starch, International Journal of Biological Macromolecules . Vol 148: 956 -968 https://doi.org/10.1016//j.ijbiomac.2020.01.181.

- Ye, J., Hu, X., Luo, S., Liu, W., Chen, J.,Zeng, Z. and Liu, C. 2017 Properties of Starch after Extrusion: A Review. Starch-Starke. Vol 70:11-12. https://doi.org/10.1002/star.201700110

- Waramboi, J.G.; Gidley, M.J.; Sopade, P.A. Influence of extrusion on expansion, functional and digestibility properties of whole sweetpotato flour. LWT- Food Sci. Technol. 2014, 59, 1136–1145. https://doi.org/10.1016/j.lwt.2014.06.016

- Huang X, Liu H, Ma Y, Mai S, Li C. Effects of Extrusion on Starch Molecular Degradation, Order–Disorder Structural Transition and Digestibility—A Review. Foods. 2022; 11(16):2538. https://doi.org/10.3390/foods11162538

- Ali, S.; Singh, B.; Sharma, S. Impact of Feed Moisture on Microstructure, Crystallinity, Pasting, Physico-Functional Properties and In Vitro Digestibility of Twin-Screw Extruded Corn and Potato Starches. Plant Food Hum. Nutr. 2019, 74, 474–480 https://doi.org/10.1007/s11130-019-00762-6

- Kaur B., Ariffin F., Bhat R., and Karim A. A., “Progress in starch modification in the last decade,” Food Hydrocolloids, vol. 26, no. 2, pp. 398–404, 2012 https://doi.org/10.1016/j.foodhyd.2011.02.016