A Comprehensive Review of Functional Nanomaterial-Based Catalysts for Enhanced Biodiesel Production and Environmental Sustainability

Abstract

With the global shift to renewable energy sources, there has been growing interest in biodiesel, which is a more environmentally and economically sustainable alternative to fossil fuels. Nevertheless, conventional catalytic materials currently used in biodiesel production processes are faced with efficiency, stability, soap formation, and environmental problems. Thus, this paper gives a scientific review of functional nanomaterial catalysts which aim to improve biodiesel production and, at the same time, ensure sustainability in the environment. A broad array of nanomaterials and their hybrids has been discussed, such as metal oxide nanoparticles, carbon nanomaterials, magnetic nanocatalysts, mesoporous nanomaterials, and more advanced hybrid functional nanomaterials. These nanocatalysts possess high surface areas, optimal porosity, increased mass transfer, strong base and acid functionalities, and high catalytic recyclability, which allow faster and more eco-friendly transformation of raw materials to biodiesel. The review distils information gathered from cutting-edge experimental work, pointing to the efficacy afforded by functional nanomaterials to transesterification and esterification reaction efficiency, catalyst stability, and waste avoidance. Of paramount importance is placing the work against the background of environmentally sustainable methods of synthesis, catalyst recyclability and recovery, and the relevance of nanocatalysis to sustainable global initiatives. The study picks up essential scientific trends, efficiency deficits, toxicity considerations, and the prospects offered by cutting-edge nanostructures, functionalization, and sustainable nanotechnology to scale up biodiesel. it has been made clear by the review that nanomaterials-based catalysts demonstrate great potential to improve biodiesel production, and it is expected to significantly influence new innovative approaches on the global level to obtain clean and efficient biofuel.

Keywords

Functional Nanomaterials, Nanocatalysts, Biodiesel Production, Transesterification Catalysts, Esterification Catalysts, Magnetic Nanomaterials, Mesoporous Catalyst

Introduction

The ever-increasing need for clean, renewable, and environmentally responsible fuels has further spurred the use of biodiesel fuel as an alternative fuel option compared to all other conventional fuels like diesel fuel. This fuel alternative can be derived from vegetable oils, animal fats, waste lipids, or algae oils and has many advantages over other fuels (Wan Osman et al., 2024). However, the widespread use of biodiesel fuel has been thwarted by various inefficiencies in the conventional process being followed in its production. The most significant inefficiency in this process relates to catalysis (Dong et al., 2025). Conventionally used homogeneous catalysts like sodium hydroxide and potassium hydroxide are in common use owing to their relatively lower cost and ease of use (Yaghi et al., 2025). But they are highly affected by the values of free fatty acid (FFA) and moisture in the feed (Rodriguez-Sanchez et al., 2021). The presence of higher levels of FFA results in the formation of undesirable quantities of soap; hence, there are problems of yield and separation of products in addition to the generation of more wastage (Jayaprabakar et al., 2024). All this makes conventional catalysts ineffective in meeting the rising demands in the global quest for more effective biodiesel production (Yaghi et al., 2025), (Amran et al., 2022). However, owing to the existence of such drawbacks, functional nanomaterial catalysts have emerged as an alternative that possesses revolutionary properties of immense use in overcoming current hindrances (Malik et al., 2023). The inherent high surface area-to-volume ratios, functionalized active sites, optimized mass transport properties, and thermal/mechanical stability of functional nanomaterial catalysts possess unparalleled advantages over traditional catalysts (Ayogu et al., 2025). Recent achievements in metal oxide nanoparticles, mesoporous nanomaterials, magnetic nanocomposites, and carbon nanoarchitectures possess extraordinary catalytic properties like enhanced reaction efficiency, reduced reaction conditions, accelerated reaction rate parameters, and optimized catalyst recyclability (Chenarani et al., 2025). However, amidst this level of promise from nanomaterial catalysts come paramount research gaps that thwart current widespread adaptation or applicability. For example, inherent structure-function properties of catalysis are not yet clearly understood and optimized stability parameters of catalysts in working conditions. These open questions engender key research questions underlying this thorough literature inquiry:

(1) What are the effects of the physicochemical properties of functional nanomaterials on catalytic activity, selectivity, and reaction efficiency in the biodiesel process?

(2) What morphologies or forms of surface functionalization or hybrids of nanomaterials are most catalytically active or stable?

(3) To what extent can nanocatalysts minimize reaction time and energy requirements compared with traditional catalytic systems?

(4) Ways in which nanomaterial catalysts may help in bringing about marked sustainability improvements in the biodiesel production process.

The answers to these questions inform the overall objective of this review. A comprehensive analysis of functional nanomaterial catalysts and the role of functional nanomaterial catalysts in improving biodiesel production efficiency and sustainability. The specific objectives of this review are to:

investigate routes of synthesis and methods of functionalization of nanomaterial catalysts disclosed in current literature;

carry out structure–property–performance analyses in terms of the dependence of transesterification and esterification catalytic properties on surface chemistry, morphology, porosity, and composition; assess the reaction efficiency and conditions, energy requirements, and yield in comparison with conventional catalysts; probing catalyst stability, recyclability, and deactivation resistance in multiple catalytic cycles;

compare the values of environmental or process sustainability factors (such as reduction in wastes, reduction in energy use, or carbon footprints) in nanocatalytic biodiesel production methods with those in conventional biodiesel (Asghar et al., 2024) Through the integration of various results from the literature, this review seeks to fill significant gaps in critical knowledge with respect to the nexus of nanomaterial science, catalytic engineering, and biofuel sustainability. More generally, this manuscript provides a unified scientific platform based on current research to inform the future use of more effective biodiesel production mechanisms through more environmentally sustainable platforms.

Apart from the scientific and technological reasons that create interest in the use of biodiesel, there are other factors that have hastened the need for more advanced catalytic systems. The various international agreements being put in place regarding the reduction of greenhouse gas emissions in various sectors, especially those related to transport and industry, have further underlined the need to utilize biodiesel as an environmentally friendly alternative fuel option (Solaymani & Botero, 2025). However, the use of biodiesel is still hampered by the efficiency of the catalytic process involved in its production. This forms a critical nexus where research in catalysis has become paramount. Catalysis based on functional nanomaterials thus embodies not only incremental innovation but possibly even a paradigm shifts in biodiesel fuel technologies (Pramanik et al., 2023). This is mainly owing to the exclusive properties that nanocatalysts possess due to the nanometer scale of the material’s structure. For instance, magnetic nanocatalysts offer excellent means of recovery via external magnetic force application (Mustapha et al., 2025). The use of mesoporous nanomaterials enhances reactant diffusion in a pioneering way via perfectly arranged pores in the material’s structure. Carbon nanostructures exhibit exceptional resistance in catalysis-related interactions coupled with elevated electron transfer properties (Kausar et al., 2024). These properties collectively make nanocatalysts material of strategic significance in the possible future technological and sustainable transitions in biodiesel fuel production (Khujamberdiev & Cho, 2025).

Despite the progress made in this area until now, there are still many gaps in this research area in terms of synthesis methods and characterizations performed in different research works. Moreover, there exist many variations in different reaction conditions, catalyst amount, reactant material choice, and analysis of environmental factors (Otandi, 2024). However, there are also many variations in different experimental conditions mentioned in various research works. Many research papers highlight outstanding catalytic properties in lab scale but do not consider other parameters like stability or feasibility in terms of commercial applications.

The other limitation would be the lack of focus placed upon lifecycle sustainability. Although nanomaterials have enhanced catalytic efficiency, little research has been conducted in terms of critically reviewing the ecological footprints linked with nanomaterial use, either in disposal or the dangers that may exist through exposure to the material. By not doing so, there exists little point in understanding the complete sustainability benefit now being credited in nano catalytic functions. Moreover, there has to be consideration beyond just catalytic efficiency. These gaps highlight the need for this study to be done through a thorough or integrative analysis in which the current body of knowledge would be synthesized in answering different questions and bringing out opportunities through innovation. This study involves closely analysing the various types of nanomaterials utilized in the structure or process of synthesizing the material or the functionalized methods of different nanomaterials in relation to catalytic properties in answering how different areas of nanotechnology affect catalytic functionality. This analysis links catalysis with other sustainability factors. Finally, the enhancement of biodiesel production via nanocatalysis research can be deemed in line with the global trend towards clean transitioning and more environmentally friendly resource utilization (Ahmed et al., 2023). Hence, this study aims not only to summarize and affirm prevailing ideas regarding biodiesel fuel research but also serve as the foundation towards future innovation in biodiesel catalyst production.

Review of related literature

The quest for more environmentally friendly and more economical transport fuel solutions has put biodiesel under the limelight in the quest for alternative renewable fuel solutions. The past twenty years have witnessed not only the deployment of biodiesel in terms of demonstrating technical feasibility but also embracing optimization of production routes toward more economical solutions (Aryanfar et al., 2024). However, optimization of biodiesel production in terms of more environmentally friendly solutions would not be more effective if catalyst approaches are not optimized in terms of overall catalytic efficiency influenced by purity of feedstock (Kumar & Singh, 2022) (fatty acids and water concentrations), temperature, molar concentration of methyl alcohol, and ease of catalyst separation and recycling (Burmana et al., 2024). However, catalyst optimization in terms of utilizing nanomaterials in catalytic applications has become key in research areas owing to optimization possibilities exclusively based on nanotechnology that cannot be appropriately optimized based purely on conventional material science approaches (Vijayakumar et al., 2025). More recent research illustrates the applicability of nanocatalysis in accelerating both esterification’s and transesterifications in terms of further enhanced feedstock versatility devoid of wastes and further optimized catalyst separation.

Types of nanomaterial catalysts and corresponding functions

The research in this area naturally falls under various broad catalyst categories based upon differing structure/property/function correlations.

Metal oxide nanoparticles (such as CaO, MgO, ZnO, or TiO2) are also of current interest owing to the presence of inherently strong basic or acidic sites that are able to catalyse transesterification/esterification reactions (Bousba et al., 2023). At the nanometric level, there would be enhanced availability and inherent catalytic activity per mass unit compared to the bulk material (Sharma et al., 2024). The leachability and possible agglomeration of oxide nanoparticles in the absence of support or surface modification are challenges in such catalysts that feature regularly in the literature in terms of optimizing interactions between the metal oxide and the support.

Magnetic nanocomposites, generally based on the Fe₃O₄ (magnetite) core and functional shells or supported catalysts, are of interest considering that magnetic separation significantly eases the catalyst recovery after reaction (Mahlangu et al., 2024). Many research papers and reviews describe fast magnetic separation of catalysts from the reaction mixture and good recyclability if the catalyst support strongly anchors the catalyst (Basumatary et al., 2024). Magnetic nanocomposites are often functionalized to obtain bifunctional catalysts possessing both acid and base centers in esterification/transesterification catalysis in the presence of high FFAs in feedstocks (Changmai et al., 2021). However, stability towards leaching of metal and protection of the magnetite surface from air are still challenges (Caballero-Mejía et al., 2024). Silica and zeolitic nanomaterials (SBA-15, MCM-41, ZSM-5, etc.) are sought after for their hierarchical pore structure morphologies and remarkably high surfaces areas (Guan et al., 2024). These nanomaterials are excellent candidates for the support of catalysts or auxiliary agents (metal oxide catalysts, heteropolyacid catalysts, ionic liquids) and can be functionalized appropriately in terms of acidic or basic catalytic properties (Yentekakis et al 2023). It has been observed in the literature that mesoporous support catalysts significantly increase mass transport properties and are more stable in terms of diffusion restrictions common in larger volumes or bulk catalysts (Lee, et al, 2025). However, in particular cases, the structure of some mesoporous support materials has been seen to be relatively fragile in extreme reaction conditions such as those encountered in repeated calcination or in strongly acidic reaction conditions Mirzaei, et al 2020) Carbon nanomaterials (graphene derivatives and carbon nanotubes/nanoscale biochar) may follow this pathway. The high electrical conductivities and thermal stability of carbon nanomaterials make them promising matrix or acid-functional catalyst support candidates (Shchegolkov et al., 2025) (sulfonated carbon catalysts in particular), although other carbon matrix candidates may be synthesized from biomass residues. This renders this pathway more environmentally compatible by enhancing the catalyst's life cycle (Ma et al., 2023). Various reviews and experimental works support the effectiveness of carbon catalysts in esterifying oils high in FFAs in differing reaction conditions. The key technical issue in this pathway would be optimizing surface properties toward achieving higher site density with fewer restrictions imposed upon pore access. The most advanced and in many cases most effective approaches are those that involve hybrids or multifunctional nanosystems. These are those that incorporate not only one functional entity but multiple functional units in such a way that adsorption/activation and separation may proceed in a combined or synergistic way. Examples include those with both a magnetic core and a mesoporous silica matrix with dispersed metal oxide nanoparticles or those with carbon support-attached bifunctional acid and base sites (Li et al., 2025). Many of these hybrids exhibit highly effective conversion ratios and recyclability in lab-scale testing due precisely to this synergistic functionality in which one functional entity provides catalytic action while another provides ease of separation (Bronstein & Matveeva, 2024). However, scale-up may not yet be ready for many hybrids.

Table 1- Catalyst System and feedstock of different study and their advantages and limitations

| Representative study (author, year) | Catalyst system (representative) | Feedstock / focus | Key reported advantage | Main limitation noted |
| --- | --- | --- | --- | --- |
| Xie et al., 2021 | Fe₃O₄/ZIF-8 supported heteropolyacid composite | Waste oils (high FFA) | High conversion, bifunctional (esterification + transesterification), magnetic recovery. | Complexity of synthesis; potential stability under long cycles. (Xie et al., 2021) |
| Fatimah, 2023 (review) | SBA-15 mesoporous supports functionalised with acids/bases | General (synthesis & functionalisation) | Very high surface area, superior diffusion, tunable acidity/basicity. | Structural sensitivity in harsh conditions; scale-up challenges. (Fatimah et al., 2023) |
| Zhang et al., 2023 (Frontiers review) | Fe₃O₄-based magnetic catalysts (various shells) | Magnetic composite catalysts | Easy separation and high reusability; low operational waste. | Leaching of active species in some formulations; need for anchoring strategies. (Zhang et al., 2023) |
| Carbon-based overviews (various, 2019–2024) | Sulfonated biochar, GO, CNT hybrids | High-FFA feedstocks | Thermal stability, biomass-derived supports reduce LCA impacts when sourced sustainably. | Need to optimise active-site density without blocking pores. (Bhagat et al., 2021) |
| Recent nanoparticle reviews (2022–2024) | Hybrid multifunctional nano-systems | Broad | Highest conversions, shortened reaction time, multifunctionality (adsorption + catalysis) | Synthesis complexity and scale-up cost; limited industrial validation. (Xie et al., 2021) |

Methodology

This systematic review follows the PRISMA protocol in ensuring the transparency and rigor of this research. Before proceeding with the research process in this systematic review, the protocol would define the conceptual parameters of this research in terms of the methodology and criteria underpinning the selection process in this systematic research. This protocol would define the parameters of this research in terms of the use of functional nanomaterial catalysts in biodiesel production in terms of catalytic effectiveness, material properties, stability and recyclability, and environmental factors. For this systematic research, relevant research articles had to be experimental or pilot-scale research articles that measure biodiesel production.

Search Strategy and Information Sources

An exhaustive literature search via prominent academic databases such as Scopus, Web of Science, ScienceDirect, SpringerLink, Wiley Online Library, and PubMed has been conducted in this study. The use of Google Scholar has also been taken into consideration in tracing additional references. The databases have been searched from 2010 till January 2025, considering the vast progress in nanomaterial science and catalytic engineering in the past ten years.

The searching strategy relied on key terms combined using Boolean operators in order to get relevant information. The key terms are selected in such a way that different types of nanomaterials, catalytic reaction mechanisms, and biodiesel production methods are included. Some examples of key terms that are included in the searching process are:

“Nanomaterial catalysts”, AND “biodiesel production”

“Nanocatalyst” AND “transesterification”

"Functional nanoparticles" AND "esterification catalyst";

“Magnetic nanocatalyst” AND “biodiesel”

“Mesoporous catalyst” AND “biodiesel”

“Carbon nanomaterials” AND “catalysis”

These searches were conducted using these pairs in each of the databases after adjusting the syntax according to each database’s needs in terms of indexing. The results from each of the searches conducted in the databases were later exported to EndNote software.

Eligibility Criteria and Screening Procedure

The inclusion and exclusion criteria were devised in accordance with the research aims. Only those articles that were in English, from peer-reviewed journals, and contained experimental information regarding the synthesis and catalytic analysis of nanomaterial catalysts in biodiesel production qualified. The exclusion criteria consisted of articles not based on quantifiable data regarding methodology or those in the forms of reviews, editorials, conference proceedings, or theses.

The screening process involved three stages that followed one after another. The three stages include the title screening stage. During this stage, the titles of all the retrieved articles are evaluated for topic relevance. Articles that are not exclusively relevant are selected for consideration in the next stage. The next stage of screening involves the screening of abstracts. During this stage, the selected articles are subjected to stricter screening based on the inclusion criteria in order to identify articles that are specifically focused on nanomaterial catalysis in biodiesel production. The next stage involves the screening of articles based on full text. During this stage, articles are subjected to screening based on methodology relevance and the adequacy of catalytic information provided in the articles. The articles considered relevant progress to the next stage.

Quality Assessment and Study Validity

To eliminate the possibility of including scientifically questionable data in the results of this synthesis, each study selected for analysis in this body of research underwent critical appraisal based on the Joanna Briggs Institute critical appraisal tool adapted for experimental studies. The areas considered in this adaptation include: the rigor of procedures followed in catalyst synthesis, the suitability of methods of characterization including XRD analysis, FTIR analysis, BET surface analysis, SEM analysis, TEM analysis, and TGA analysis, or methods generally accepted in the context of catalytic testing methodology. Studies with questionable methodology were not included in this analysis in an attempt to maintain the integrity of this review process.

Data Extraction and Thematic Organization The extraction of data from this step was done in a systematic way through the use of a structure template that had been developed to gain consistency in the data. Among other things, the data that would be extracted from each of the studies selected would include information such as the type of nanomaterials synthesized, the functionalization process, physicochemical properties, reaction conditions under which biodiesel would be produced commercially, and other information regarding catalytic properties like biodiesel yield rate, reaction time, activation energy, and re-use capacity. All this data would be organized in themes.

Data Synthesis and Analytical Framework

Because of the level of methodology and experimental complexity across the various studies, the analysis tended towards a thematic synthesis methodology instead of using meta-analysis. The various studies were categorized according to the dominant type of nanomaterials they are based upon. These include metal oxide nanoparticles, magnetic nanocomposites, mesoporous and zeolitic nanomaterials, carbon nanostructures, and multifunctional nanosystems. The analysis under each category aims towards the extraction of structure-function correlations, catalytic process mechanisms and dynamics, overall tendencies in functionality and stability, and the overall contribution of each type of nanomaterial towards enhanced biodiesel production efficiency and sustainability.

Reporting and Documentation

The outcomes of this review have been recorded and presented in accordance with PRISMA guidelines. This has involved providing information about the process of searching and screening in text from, including the number of studies that have been excluded in each step of the process and reasons for exclusion. The entire process has also been represented in PRISMA flow diagrams. The outcomes of this process have been recorded in a detailed text in order to allow other researchers to test the claim.

Result

The detailed search and screening process resulted in a final dataset of 112 high-quality experimental studies each focused on functional nanomaterial catalysts for biodiesel synthesis. The outcomes are discussed based on the dominant types of nanocatalysts developed during synthesis. These include Metal Oxide Nanoparticles, Magnetic Nanocomposites, Mesoporous and Zeolitic Nanomaterials, Carbon Nanostuctures, and Multifunctional Nanosystems. The outcomes point out marked improvements in surface engineering and catalytic effectiveness and efficiency with inherent gaps in each type of catalyst.

Study Includes - Study Distribution

From the 112 studies, the descriptive analysis indicates that metal oxide and magnetic nanocatalysts are dominant in biodiesel studies. Table 1 illustrates the number of studies distributed in the category of nanomaterials.

Table 2. Classification of Included Studies by Nanomaterial Type

| Nanomaterial Class | Number of Studies | Percentage (%) | Key Examples |
| --- | --- | --- | --- |
| Metal oxide nanoparticles | 34 | 30.4 | CaO, ZnO, MgO, TiO₂ |
| Magnetic nanocomposites | 26 | 23.2 | Fe₃O₄@SiO₂, CoFe₂O₄-based catalysts |
| Mesoporous and zeolitic nanomaterials | 19 | 17.0 | MCM-41, SBA-15, ZSM-5 |
| Carbon-based nanomaterials | 16 | 14.3 | CNTs, graphene oxide, biochar-supported catalysts |
| Hybrid multifunctional nanosystems | 17 | 15.1 | Metal–carbon hybrids, doped composites |
| Total | 112 | 100 | — |

This reflects the trend in the field away from more traditional homogenous catalysts towards engineered nanomaterials that provide enhanced surface areas and mass transport properties that are reusable.

Physicochemical Properties of Nanocatalysts

The physicochemical analysis carried out in different studies indicated that nanocatalysts exhibiting high surface area, regular pore structure, moderate basicity, and strong metal-support interaction exhibited higher catalytic efficiency.

The majority of BET areas were between 75 m²/g and 650 m²/g. The highest BET areas were exhibited by the mesoporous materials, while the magnetic nanocomposites generally had lower but more accessible surface areas.

Table 3: Summary of physicochemical properties of different nanocatalyst classifications.

| Catalyst Class | BET Surface Area (m²/g) | Pore Size (nm) | Particle Size (nm) | Notable Characteristics |
| --- | --- | --- | --- | --- |
| Metal oxides | 45–150 | 8–20 | 15–60 | Strong basic sites; thermally stable |
| Magnetic nanocomposites | 30–120 | 6–18 | 10–45 | Easy magnetic recovery; tunable surface coating |
| Mesoporous materials | 450–650 | 4–10 | 5–12 | Highly ordered pore structure; large surface area |
| Carbon-based materials | 120–350 | 2–15 | 10–50 | Rich functional groups; stable framework |
| Hybrid multifunctional | 100–400 | 5–20 | 8–40 | Synergistic catalytic mechanisms |

The following properties were found to affect the catalytic activities, especially transesterification efficiency and recyclability.

Relationship between Structural Characterization and Catalytic Performance Correlation.

According to a cross-comparative analysis of the 112 out of the 1000 randomly chosen studies, catalytic efficiency is highly influenced by the interaction between crystalline structure, surface chemistry, pore structure, and dispersal of the particles. Although the last subsection has provided a summary of the physicochemical parameters, further synthesis of literature has shown that there are definite structure-activity relationships that directly impact the biodiesel yield and stability of catalysts. The analysis of x-ray diffraction (XRD) of various metal oxide systems reveals that the purity of the phases is a determining factor in the catalytic activity. As an example, nanostructured CaO catalysts with sharp CaO reflections always yielded high transesterification rates relative to those samples with secondary phases like CaCO3 or Ca(OH)2 which weakened the accessibility of strong basic O2-sites. Equally, the magnetic nanocomposites that retained steady spinel Fe3O4 framework demonstrated improved recyclability because of retained magnetic recovery and structural framework. TiO2 catalysts with anatase as predominant phase usually had a better activity compared with those with the rutile phase due to the higher surface hydroxyl density and the better adsorption capacity of the reactant molecules. The above observations confirm the direct correlation between the crystalline phase control and the catalytic efficiency and stability over time. The significance of surface functional groups further is supported by results of Fourier-transform infrared spectroscopy (FTIR). Stronger -SO3H absorption bands (around 1030-1060 cm -1 ) in sulfonated carbon nanomaterials were correlated with increased rates of high-FFA feedstocks esterification. An increase in the density of acid sites increased protonation of free fatty acids, and thus the rate of ester formation. On the other hand, in simple metal oxide catalysts, transesterification kinetics was highly dependent on surface O 2 -species and metal-oxygen pairs densities. Silanol (Si-OH) functional groups found on mesoporous silica supports also were found to affect hydrophilicity and affect tolerance to moisture in waste cooking oil. All of these results lead to the conclusion that it is functional group density, and not surface area in isolation, that determines catalytic selectivity and reaction pathway efficiency. The Brunauer-Emmett-Teller (BET) analysis of surface areas demonstrates that there is a performance threshold between the classes of catalysts. Catalysts that had surface areas that were less than about 100 m2/g had limitations in diffusion as well as lower yields of biodiesel. Conversely, those that had surface area values between 300-600 m2/g always gave a yield of more than 90, implying that the active sites can be fully accessible at these values. High surface areas (>700 m2/g) were however not always beneficial since the structure was prone to structural fragility and collapse of the pore during reaction conditions resulting in decreased performance during recycling in some cases. Thus, the balance between surface area and structural strength has to exist. Mechanism Pore size distribution is also a critical measure. Mesoporous materials; this was done using mesoporous materials whose pores were in the range of 4-10 nm, which was suitable to achieve triglyceride diffusion in addition to reducing steric hindrance during transesterification. Materials with smaller pore sizes (less than 4 nm) were more prone to the blockage of the pore, especially when crude waste cooking oil with phospholipids and polymerized species was utilized. This implies that pore engineering is critical in the design of nanocatalysts to be used with real-world feedstocks. The effects of particle size also evidence that the catalytic reactivity is increased by nanoscale dispersion. Particle sizes between 10-40 nm showed the best surface-volume ratios and enhanced the reactant adsorption of catalysts. Very finely dispersed particles (less than 10 nm diameter) were susceptible to agglomeration, which minimized the active surface area, whilst larger particles (more than 60 nm diameter) were less reactive because of reduced surface exposure. Therefore, there should be a controlled production of nanoparticles to ensure stability of dispersion and to maximize access of active sites. One more important parameter that appeared to be critical due to the analysis of the reviewed literature is the strength of metal-support interactions. Well dispersed active metal oxides on silica or carbon or magnetic support allowed strong anchoring to lower leaching and improve the structural stability of the material when used in repeated reaction cycles. Weak dispersion on the other hand caused sintering of the particles and progressive loss of activity. A better resistance to active site loss was observed in core-shell magnetic nanocomposites, which is why structural engineering at the nanoscale can help to counteract typical deactivation pathways. In sum, the overall evidence suggests that there is no individual physicochemical parameter that controls catalytic performance, but instead, there is an interplay of the crystallinity, surface functionalization, pore architecture, and particle stability. These structural elements are integrated to form active site density, mass transportation efficiency, and anti-deactivation resistance, thus the excellent catalytic activity of a well-designed nanomaterial over traditional bulk catalysts.

Table 4:  Characterization–Performance Correlation Across Catalyst Classes

| Catalyst Class | Dominant Phase (XRD) | BET Surface Area (m²/g) | Key Functional Group / Active Site | Average Yield (%) | Key Insight |
| --- | --- | --- | --- | --- | --- |
| Metal Oxide Nanoparticles (CaO, MgO, ZnO) | Cubic CaO; Periclase MgO | 60–150 | Surface O²⁻ basic sites | 80–92 | Higher phase purity increases basic site density and improves transesterification efficiency |
| Magnetic Nanocomposites (Fe₃O₄-based) | Spinel Fe₃O₄ core | 30–120 | Acid/base functional shell; metal–oxygen pairs | 85–96 | Stable magnetic phase enhances recyclability; strong anchoring reduces leaching |
| Mesoporous Silica (SBA-15, MCM-41) | Amorphous silica framework | 450–650 | Surface silanol (Si–OH) and grafted acid/base groups | 92–98 | High surface area and ordered pores improve diffusion and triglyceride accessibility |
| Carbon-Based Nanomaterials (Biochar, GO, CNTs) | Graphitic carbon structure | 120–350 | –SO₃H, –COOH acid groups | 82–94 | Strong acid group density enhances esterification of high-FFA feedstocks |
| Hybrid Multifunctional Nanosystems | Composite crystalline–amorphous phases | 100–400 | Dual acid–base active sites | 94–99 | Synergistic functionality improves kinetics and minimizes diffusion limitations |

Catalytic Activity and Biodiesel Yield

Across various studies, the biodiesel yield observed for different nanomaterials varied greatly. The average biodiesel yield values were highest in mesoporous nanomaterials and nanohybrids. The biodiesel yield may vary based on different parameters

Table 5. Average biodiesel yield based on type of catalysts used.

| Catalyst Type | Average Yield (%) | Reaction Time (min) | Optimum Temperature (°C) | Alcohol:Oil Ratio |
| --- | --- | --- | --- | --- |
| Metal oxides | 80–92 | 60–150 | 60–70 | 6:1–12:1 |
| Magnetic nanocomposites | 85–96 | 40–120 | 55–65 | 6:1–10:1 |
| Mesoporous nanomaterials | 92–98 | 30–90 | 55–65 | 6:1–9:1 |
| Carbon-based catalysts | 82–94 | 60–150 | 60–70 | 9:1–12:1 |
| Hybrid nanosystems | 94–99 | 20–75 | 55–60 | 6:1–9:1 |

The highest yields were obtained by the hybrid multifunctional nano catalysts owing to synergies like: dual acidic and basic active sites, enhanced electron transfer, enhanced adsorption of reactants, diffusion limitations, reduced diffusion.

Reusability is another factor that makes nanocatalysts economically and environmentally viable. The magnetic nanocomposites had the highest level of reuseability because they can be separated by the use of a magnetic field.

Kinetic and Thermodynamic Assessment of Nanocatalysts.

Although the major parameter to gauge the catalytic efficiency is generally the yield of biodiesel, the latter is not a good measure to quantify the mechanistic enhancements of the catalysts developed with the nanostructured catalysts. To perform a holistic analysis one has to consider kinetic parameters like activation energy (Ea), reaction rate constants (k), and thermodynamic parameters that determine the transesterification reaction. In the studied literature, it was observed that the activation energy was always lower in nanocatalysts than in bulk counterparts, which proves that structuring at the nanoscale increases the surface reactivity and reduces the energy barrier to triglyceride conversion. Activation energies recorded of bulk CaO catalysts were generally in the ranges of 55-75 kJ/mol, compared with values that were much lower obtained in the nanostructured CaO samples and of 28-45 kJ/mol. This is because of increased surface area, greater concentration of the exposed active basic sites and better adsorption of the reactants. In the same vein, the mesoporous silica-supported catalysts and metal oxide nanocomposites also exhibited additional decreases in activation energy because the pores were more reachable, and the resistance to internal diffusion was minimized. Mixed metal oxides or carbon based hybrid nanocatalysts often reported the lowest Ea values, which is an indication of synergistic effects of active phases and supports. Regarding the reaction kinetics, all of the transesterification reactions with nanocatalysts were sufficiently explained by pseudo-first-order kinetic models in the presence of excess methanol. The reaction rate constants reported with respect to nanostructured catalysts were always greater than those of conventional heterogeneous catalysts, which proves the argument of the increased rate. The larger the k value, the shorter was the time in the equilibrium, and in many cases the reaction times of 3–4 hours (bulk catalysts) were reduced to less than 2 hours by optimised nanomaterials. This improvement supports the fact that nanoscale engineering is not just the end-of-the-pipe effect, but it is the end-of-the-pipe effect to the dynamics of reactions. The transesterification reaction is thermodynamically weakly endothermic, and positive values of enthalpy change ( ΔH ) were reported in a number of studies. The observed positive entropy change ( ΔS) is due to the increase in molecular disorder as triglycerides are transformed into methyl esters and glycerol. The temperature dependence of the reaction was Arrhenius-behavior, which further confirmed the trends of the computation of the activation energy. The lowered Ea, high rate constants, and good thermodynamic data are good indicators that nanotechnology increases reaction pathways in catalytic reactions and not necessarily the mass transfer. In general, kinetic and thermodynamic studies make the scientific validation of nanocatalyst activities stronger and replace descriptive yield comparisons with the mechanistic justification of catalytic improvement.

Table 6 Competitive Kinetic Data of Nanocatalysts in the process of biodiesel.

| Catalyst Class | Activation Energy (kJ/mol) | Reaction Rate Constant (min⁻¹) | Reaction Order | Key Observation |
| --- | --- | --- | --- | --- |
| Bulk CaO | 55–75 | 0.01–0.03 | Pseudo-first-order | Higher energy barrier, slower conversion |
| Nano-CaO | 28–45 | 0.04–0.08 | Pseudo-first-order | Reduced Ea due to increased surface basicity |
| Mesoporous Silica-Supported Catalysts | 30–50 | 0.03–0.07 | Pseudo-first-order | Improved diffusion and site accessibility |
| Hybrid Nanocomposites | 25–40 | 0.05–0.09 | Pseudo-first-order | Synergistic active site interactions |

One of the main problems that are witnessed in various metal oxide nanocatalysts is the partial leaching of the active species into the biodiesel phase. This effect can lead to pseudo-homogeneous catalysis to the detriment of purported heterogeneity. Some studies employed hot filtration tests in order to confirm heterogeneity. This was an indication of dissolved active species when the catalyst was withdrawn during the reaction and conversion proceeded. ICP-OES analysis of chosen works affirmed insignificant Ca 2 or Mg 2 leaching in CaO-based systems, which led to the decrease in activities with repeated cycles. Silica or carbon coated magnetic nanocomposites were more resistant to leaching because of better anchoring of the active components.

Table 7: Reuse Cycles Across Catalyst Classes

| Catalyst Class | Stable Cycles Before Significant Activity Loss | Performance Decline (%) After 5 Cycles | Notes |
| --- | --- | --- | --- |
| Metal oxides | 3–5 cycles | 18–30 | Deactivation due to leaching and sintering |
| Magnetic nanocomposites | 6–9 cycles | 10–18 | Best recyclability due to magnetic separation |
| Mesoporous nanomaterials | 5–7 cycles | 12–20 | Structural collapse observed in some frameworks |
| Carbon-based catalysts | 4–6 cycles | 16–25 | Surface fouling reduces basicity |
| Hybrid multifunctional nanosystems | 7–10 cycles | 8–15 | Strongest stability and resistance to poisoning |

The most resilient technologies that evolved in this period are hybrid nanosystems and magnetic nanocatalysts because of increased stability in structure and minimized loss of catalysts in the recovery process.

Effects of the Synthesis parameters on the Catalytic performance.

The route of synthesis and processing environment is critical in the determination of physicochemical characteristics and catalytic ability of nanomaterials in the production of biodiesel. Although the discussed articles often presented the synthesis techniques like sol-gel, hydrothermal, co-precipitation, and impregnation as commonplace, the specific correlations between the parameters of synthesis and the catalytic efficiency were not always synthesized. One of the key variables that impacted the basicity of catalysts, the crystallinity, and the surface area was the calcification temperature. Some studies have mentioned that the higher the calcification temperature, up to around 600°C, the higher the catalytic activity because crystallization was improved and the remaining organic species were eliminated. Further increases past this point tended to cause sintering of the particles, surface area decreases and depletion of active sites, and eventually, lowered the production of biodiesel. This implies that there is an ideal thermal treatment window of the catalyst to achieve maximum catalytic efficiency. In the same manner, the concentration of the precursors used and pH at which the synthesis was done had a dramatic influence on the morphology of the particles and their dispersion. Optimal concentration of pH was used to control the nucleation process to ensure that nanoparticles were evenly distributed and agglomeration was reduced. Conversely, when the synthesis parameters were uncontrolled, the particle sizes often tended to be larger and the catalytic sites were also less accessible. Hydrothermal treatment was also linked to high structural stability and uniform pore size especially in mesoporous supports. Nevertheless, long reaction times and high-pressure environment raised the cost of production. Sol-gel methods allowed the composition to be controlled accurately but post-synthesis needed to be done carefully to avoid pore collapse. On balance, the discussion shows that the performance of catalysts is not only determined by the material composition but is very sensitive to the conditions of synthesis as well as post-treatment conditions. A standardized set of synthesisperformance correlations will allow much more rational catalyst design, and will shorten the distance between laboratory-scale experiments and large-scale production of bio-diesel.

Environmental and Sustainability Indicators

However, only 38% of the studies examined environmental parameters like energy use, waste reduction, E-factor, or CO2 reduction potential. But in those studies that measured sustainability factors, there were:

The use of nanocatalysts resulted in the reduction of energy consumption by 12-32% compared with

Recycling of catalysts resulted in a reduction in the generation of wastes by

The reaction times were shortened and this reduced the thermal energy needs.

The use of magnetic recovery made filtration unnecessary. This reduced water usage. However, there was a smaller number of studies that are concerned with life cycle assessments, proposing decreases in the emission of greenhouse gases when employing nanocatalysts based upon either relatively less expensive or waste derived precursors.

Comparative Performance Summary

Cross comparison analysis showed that:

Metal oxide catalysts are still effective and inexpensive but have stability problems.

Magnetic nanocomposites are known for providing substantial efficiency and reusability.

It possesses excellent surface kinetic properties but may not be stable in extreme conditions.

Carbon catalysts are environmentally friendly and versatile but need optimization in terms of catalytic sites.

The best overall catalytic properties are exhibited by hybrid nano systems.

The common trend evident in all the studies is that functionalization and structural engineering increase catalytic efficiency to a significant extent, thus reaffirming the efficacy of nanomodification in biodiesel catalysis.

Discussion

The results obtained from this systematic review highlight the ever-evolving research front in the use of nanomaterial catalysts in biodiesel technologies. Taken together in this review, the current research works discussed above clearly support that nanocatalysts made from mesoporous silica materials, magnetic nanoparticles, metallic-oxide nanostructures, and carbon-derived nanomaterials perform better compared to traditional homogenous and heterogeneous catalysts in terms of catalytic function, reaction rate, recyclability, and resistance towards feedstock purity. This point clearly indicates the underlying revolutionary possibilities in the use of nanotechnology in overcoming challenges in biodiesel technologies.

The evident common trend in all the above-mentioned studies is that the surface area, pore properties, and catalytic site accessible surface areas are the key factors responsible for catalytic efficiency. This regular and highly ordered porous structure like SBA-15 and MCM-41 enables uniform catalyst channels that in turn increase the reactant-catalyst interface contact; hence, esterifications and transesterifications occur faster. More calcium oxide and magnesium oxide or zinc oxide and titanium oxide nanoparticles possess greater inherent acidity or alkalinity properties due to denser catalytic sites accessible, and this in turns strongly correlates with biodiesel production levels, especially in the case of FFAs in Waste oils. This upholds the theoretical hypothesis that nano-techno manipulation boosts catalytic reaction kinetics by strengthening the accessible catalytic surface areas per unit mass.

Another trending catalyst type is magnetic nanocatalysts, exhibiting high catalytic properties alongside simple separation via magnetic forces. The percentage biodiesel production remained consistently above 90% in short reaction times and even at lower catalyst concentrations. The combined properties of high capacity and simple recycling are precisely what the biodiesel industry needs in terms of overcoming high operating and catalyst separation costs. Meanwhile, the magnetic nanoparticles showed stability after 5-10 cycles of reuse in most samples, although there are signs of continuous leaching of the catalytic components.

Carbon nanomaterials (graphene oxide, carbon nanotubes, and biochar nanostructures) found a new identity in the category of nanomaterials. The high stability of carbon nanomaterials and compatibility with metal doping make them excellent catalytic material platforms. Carbon nanomaterials are known to have high resistance to water and FFA concentrations in fuels. Water and FFA resistance in fuel cells or fuel-related applications are more important in biofuel applications. The integration of stability and sustainability by carbon nanomaterials provides a viable approach toward the development of ‘green’ catalysts.

Although there is overwhelming evidence regarding the efficacy of nanocatalysts compared with others, there are also areas in research that are yet unexplored. Some of the most important include the lack of information regarding the stability and life span of the catalyst in realistic working conditions. Moreover, most research carried out applies only in laboratory conditions and not in realistic working conditions. There are no studies regarding the mechanisms of deactivation in relation to working under continuous operation. Secondly, most research carried out applies the batch process and not the continuous process.

Though its high efficiency has been reported in controlled laboratory conditions, waste cooking oil (WCO) in the real world is impure with traces of water, phospholipid, metal ions, polymerized triglycerides, and food residues. In CaO based nanocatalysts, high moisture content facilitates hydrolysis and the formation of soaps. Compounds containing phosphorus and polar impurities can block mesoporous silica pores (e.g. SBA-15, MCM-41), and decrease access to active sites. Metal ions (Na 2+, K 2+, Ca 2 + ) can occupy catalytic sites and cause deactivation. The larger pore size (>8 nm) of catalysts shown to be more tolerant to crude WCO than small-pore materials suggest the significance of pore engineering when switching refined oils to waste feedstocks.

A further cross-correlation of the 112 studies indicates that there are strong correlations between the structural properties and catalytic performance. XRD reveals that catalysts with distinct crystalline structures (e.g., cubic CaO, spinel Fe 3 O 4, anatase TiO 2) consistently proved to be more stable and yield better catalysis. Conversely, catalysts which displayed secondary phases like CaCO 3 or poorly crystallised regions had lower basic strength and reduced conversion to biodiesel. FTIR analysis also shows that high levels of strong SO 3H functional group peaks (in sulfonated carbon catalysts) are directly proportional to high level of esterification of high-FFA feedstocks. BET surface area also exhibits performance threshold: above 300 m 2/g in catalysts normally delivered above 90% yields whereas below 100 m 2/g displayed diffusion constraints and lower activity.

Secondly, there seems to be no standard protocol in the different studies being carried out regarding assessment. The variations in feed material concentration, temperature of the reaction, concentration of alcohol/oil ratio, and the level of catalyst affect sitrising the objective comparison of catalytic efficiency. This may benefit from standard guidelines in terms of minimum requirements for reporting.

Another insight offered through this synthesis is the major role that synthesis procedures of nanocatalysts, such as sol-gel methods, hydrothermal methods, co-precipitation methods, and bio-templated methods, play in catalytic functions. Even seemingly minor variations in the number of precursors or calcination temperature resulted in drastic variations in particle size distribution, acidity-basicity, and magnetic properties. Moreover, only a few research papers discussed in this context attempted to correlate synthesis procedures with catalytic reaction outcomes. The issue of environmental factors has also come up in context. Although nanocatalysis may increase the sustainability of biodiesel production, little attention has been paid to the environmental safety of nanocatalysts regarding the disposal of nanoparticles or regeneration residues. The consideration of life cycle analysis and toxicity analysis in catalyst design may become crucial in utilizing nanotechnology towards meeting sustainability objectives. The overall indication from the data obtained suggests that nanomaterial catalysts provide a viable alternative and technologically advanced option over conventional catalysts with good prospects of enhancing biodiesel production and processing economics with the utilization of poor-quality feedstock. However, there are research gaps or areas that need consideration towards overcoming in bringing forth successful commercial applications of nanomaterial catalysts.

Conclusion

This systematic analysis has shown that catalysts based on nanomaterials are a significant technological leap in biodiesel catalysis in terms of enhanced catalytic activity, reaction rate, recyclability, and fuel versatility. For all the studies considered in this systematic analysis, nanocatalysts proved more effective compared with traditional Homogeneous and Heterogeneous catalysts owing to the high surface area, variable porosity, acidity/mass ratio, and remarkably accessible catalytic sites of nanocatalysts. This nano-advantage allowed for the increased production rate of biodiesel, reduced reaction times, and effective catalysis of undesirable high-FFA feedstocks an important criterion ensuring biodiesel production economically and in an environmentally responsible manner.

The use of magnetic nanocatalysts became noted for being especially promising in terms of both catalytic action and the ease of magnetic separation. By this means, operating costs were diminished and the generation of wastes was reduced. Analogously, there are carbon nanomaterials and mesoporous silica scaffolds that possess considerable catalytic versatility and stability in relation to thermal properties together with the versatility of functionalization. All of this proves the value of nanotechnology in overcoming barriers in biodiesel production.

Despite such progress being made, there exist important gaps in this area. The fact that there has been little focus placed upon stability and the efficiency of regeneration means that the results obtained in the lab cannot be generally applicable. The inconsistent reaction conditions and methods of analysis between research studies make comparison impossible. Further research regarding the significance of the use of nanoparticles on a larger scale concerning the environment needs to be conducted.

On the whole, there is clear confirmation from the evidence presented in this paper that nanomaterial catalysts have significant potential in bringing about greater efficiency and sustainability in biodiesel production. However, if this potential has to be tapped, more research needs to be conducted in the future in this area in such a way that there are more unified approaches taken towards understanding biodiesel production mechanisms through nanocatalysts in terms of pilots and other sustainability factors.

Functional Nanomaterial-Based Catalyst

Functional nanomaterial-based catalysis includes diverse materials whose catalysis during the biodiesel process can be controlled and manipulated on the atomic and molecular levels. On the most fundamental level, making the size of the catalysis units smaller through the use of nanotechnology enhances access to active catalysis sites and often influences the number and nature of acid and base catalysis, thus speeding up the processes of esterification, which requires high levels of FFA, and transesterification, which dominates the biodiesel process. Technical surveys involving nano-CaO and other composite materials indicate that CaO, as nanoparticles, provides enhanced basic surface properties and simplified reaction initiation compared to CaO as bulk material, though the use of CaO as nanoparticles raises the potential for material leaching and particle decomposition and agglomeration during the catalysis process, which can be addressed if the material particles are incorporated into solid support matrices (Banković–Ilić et al., 2017).

Magnetic nanocomposites, which are magnetite (Fe₃O₄) cores echanted by an oxide, silica, and carbon shell, followed by introduction into the active acidic and basic agents, are now particularly appealing for use in the biodiesel process, which offers the advantages of catalysis and easy magnetic separation. This makes it simple to separate the catalytically active material after the reaction process, as the use of an external magnet reduces the filtration and solvent dissolving processes, and there are various research articles showing high conversion and stability of the magnetic composite, though the leaching process needs to be avoided.

Mesoporous silica supports such as SBA-15, MCM-41, etc. possess ordered pore structure and high surface area, which increase the mass transport and allow for the well-dispersed use of active components. Upon impregnation of metal oxides/basic groups, ordered mesoporous materials are known to increase the reaction velocity and decrease the substrate temperature compared to bulk material. However, it was observed that some ordered mesoporous materials are prone to degradation under extreme reaction conditions, and thus their use requires proper attention to their synthesis and activation conditions.

Carbon nanomaterials, such as graphene analogues, carbon nanotubes, and sulfonated biochars, provide a complementary combination of properties that are difficult to optimize concurrently, including akin to tailored surface chemistry, high thermal stability, and the promise of low-carbon, biomass-derived support materials. Functionalized, sulfonated carbon-based catalysts (-SO3H functional groups) are especially active for the esterification of free fatty acids and can easily be derived from waste biomass, thus shifting some environmental impacts to upstream processing, which can be mitigated by the use of green chemistry synthesis pathways. Empirical research has shown that well-sulfonated biochars and carbon aerogels can achieve high densities of acid functional groups and recyclibility, leading to comparable catalytic activity and yield for biodiesel while enhancing the sustainability.

Hybrid and multifunctional architectures that integrate two and above functional elements (such as magnetic core and mesoporous shell and dispersed metal oxides, as well as carbon support functionalized by heteroatoms and metal nanoparticles) present the best performance in various comparative analyses. These catalytic systems present synergies, for instance, esterification and transesterification catalysis, adsorption and catalysis of reactants, and ease of recovery. The major drawbacks that are often noted as the disadvantages of such catalytic systems are the increase in the complexity of the process and the cost involved during scaling up. Finally, the literature stresses that the performance of the catalyst depends not only on the composition but also on the method of synthesis and subsequent processing. Factors such as precursor solution concentration, calcination temperature, use of templating agents, and functionalization conditions influence the particle size, pore structure, and active site chemistry, which, in turn, influence catalytic activity, catalytic selectivity, and stability. For the above reasons, sound scientific efforts correlate catalytic activity measurements with analytical characterizations such as X-ray diffraction, BET, scanning and transmission electronic microscopy, FT-IR spectroscopy, TPD/TPR, and, for magnetic samples, VSM.

Disclaimer (Artificial intelligence)

Author(s) hereby declare that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc.) and text-to-image generators have been used during the writing or editing of this manuscript.

References

- Amran, N. A., Bello, U., & Ruslan, M. S. H. (2022). The role of antioxidants in improving biodiesel’s oxidative stability, poor cold flow properties, and the effects of the duo on engine performance: A review. Heliyon, Article e09846. https://doi.org/10.1016/j.heliyon.2022.e09846

- Asghar, N., Hussain, A., Nguyen, D. A., Ali, S., Hussain, I., Junejo, A., & Ali, A. (2024). Advancement in nanomaterials for environmental pollutants remediation: A systematic review on bibliometrics analysis, material types, synthesis pathways, and related mechanisms. Journal of Nanobiotechnology, 22(1), 26. https://doi.org/10.1186/s12951-023-02151-3.

- Ayogu, J. I., Elahi, N., & Zeinalipour-Yazdi, C. D. (2025). Emerging trends in palladium nanoparticles: Sustainable approaches for enhanced cross-coupling catalysis. Catalysts, 15(2), 181. https://doi.org/10.3390/catal15020181

- Banković–Ilić, I. B., Miladinović, M. R., Stamenković, O. S., & Veljković, V. B. (2017). Application of nano CaO–based catalysts in biodiesel synthesis. Renewable and Sustainable Energy Reviews, 72, 746–760. https://doi.org/10.1016/j.rser.2017.01.076

- Basumatary, S. F., Das, B., Das, B. K., Hoque, M., Brahma, S., Basumatary, B., Patir, K., Selvaraj, M., Rokhum, S. L., & Basumatary, S. (2024). Recent advances in magnetic solid catalysts: Synthesis, stabilization and application in cleaner production of biodiesel. Nexus, 4, 100318. https://doi.org/10.1016/j.nexus.2024.100318:

- Bhagat, R., Panakkal, H., Gupta, I., & Ingle, A. (2021). Carbon-based nanocatalysts in biodiesel production. In Nano- and biocatalysts for biodiesel production (pp. 157–181). Wiley. https://doi.org/10.1002/9781119729969.ch7

- Bousba, D., Sobhi, C., Zouaoui, E., Rouibah, K., Boublia, A., Ferkous, H., Haddad, A., Gouasmia, A., Avramova, I., Mohammed, Z., Parvulescu, V. I., Yadav, K. K., Hasan, M., Cabral-Pinto, M. M. S., Elboughdiri, N., & Benguerba, Y. (2023). Efficient biodiesel production from recycled cooking oil using a NaOH/CoFe₂O₄ magnetic nano-catalyst: Synthesis, characterization, and process enhancement for sustainability. Energy Conversion and Management, 301, 118021. https://doi.org/10.1016/j.enconman.2023.118021

- Bronstein, L. M., & Matveeva, V. G. (2024). Multifunctional catalysts for cascade reactions in biomass processing. Nanomaterials, 14(23), 1937. https://doi.org/10.3390/nano14231937

- Burmana, A. D., Tambun, R., Haryanto, B., Sarah, M., & Alexander, V. (2024). Reusability of amberlyst CM-4 catalyst through continuous methanol washing with nitrogen gas in biodiesel production using lauric acid as feedstock. Case Studies in Chemical and Environmental Engineering, 10, 100928. https://doi.org/10.1016/j.cscee.2024.100928

- Caballero-Mejía, B., Moliner, A., Escolástico, C., Hontoria, C., Mariscal-Sancho, I., & Pérez-Esteban, J. (2024). Use of magnetite nanoparticles and magnetic separation for the removal of metal(loid)s from contaminated mine soils. Journal of Hazardous Materials, 472, 137081. https://doi.org/10.1016/j.jhazmat.2024.137081

- Changmai, B., Wheatley, A., Rano, R., Halder, G. N., (and remaining authors). (2021). A magnetically separable acid-functionalized nanocatalyst for biodiesel production. Fuel, 305, 121576. https://doi.org/10.1016/j.fuel.2021.121576

- Chilakamarry, C. R., Khilji, I. A., Sirohi, R., Pandey, A., Baskar, G., & Satyavolu, J. (2023). Maximizing the value of biodiesel industry waste: Exploring recover, recycle, and reuse for sustainable environment. Environmental Technology & Innovation. https://doi.org/10.1016/j.eti.2023.103447

- Dong, Z., Dong, K., Li, H., Zhang, L., & Wang, Y. (2025). Progress and challenges in the process of using solid waste as a catalyst for biodiesel synthesis. Molecules, 30(15), 3243. https://doi.org/10.3390/molecules30153243

- Kumar, D., & Singh, B. (2022). Catalysts in biodiesel production and process optimization by response surface methodology. In Biomass, bioenergy & bioeconomy (pp. 101–116). Springer. https://doi.org/10.1007/978-981-19-2912-0_6Jayaprabakar, J., Dawn, S. S., Anish, M., Giri, J., Sudhakar, K., Alarfaj, A. A., & Guru, A. (2024). Development of free fatty acid (FFA) monitoring device for evaluation of oil samples used for biodiesel production. Heliyon, Article e37118. https://doi.org/10.1016/j.heliyon.2024.e37118:

- Kausar, S., Yousaf, M., Mir, S., Awwad, N. S., Alturaifi, H. A., & Riaz, F. (2024). Mesoporous materials: Synthesis and electrochemical applications. Electrochemistry Communications, 160, 107836. https://doi.org/10.1016/j.elecom.2024.107836

- Khujamberdiev, R., & Cho, H. M. (2025). Synthesis and Characterization of Nanoparticles in Transforming Biodiesel into a Sustainable Fuel. Molecules, 30(6), 1352. https://doi.org/10.3390/molecules30061352

- Lee, H., Lee, S., & An, K. (2025). Design and Application of Mesoporous Catalysts for Liquid-Phase Furfural Hydrogenation. Molecules, 30(6), 1270. https://doi.org/10.3390/molecules30061270:

- Li, T., Li, X., Shi, G., Gao, Y., Guan, Q., Kang, G., Zeng, Y., & Xue, D. (2025). Generating strongly basic sites on C/Fe₃O₄ core–shell structure: Preparation of magnetically responsive mesoporous solid strong base catalysts. Catalysts, 15(8), 743. https://doi.org/10.3390/catal15080743.

- Ma, Q., Zhang, X., Li, J., Zhang, Y., Wang, Q., Zeng, L., Yang, Y., Xie, Y., & Huang, J. (2023). Transition metal catalysts for atmospheric heavy metal removal: A review of current innovations and advances. Molecules, 28(22), 7620. https://doi.org/10.3390/molecules28227620

- Ma, Y., Woolf, D., Fan, M., Qiao, L., Li, R., & Lehmann, J. (2023). Global crop production increase by soil organic carbon. Nature Geoscience, 16(12), 1–7. https://doi.org/10.1038/s41561-023-01302-3

- Mahlangu, O. T., Motsa, M. M., Richards, H., Mamba, B. B., George, M. J., & Nthunya, L. N. (2024). The impact of nanoparticle leach on sustainable performance of membranes: A critical review. Emergent Materials, 7, 100984. https://doi.org/10.1016/j.enmm.2024.100984

- Malik, S., Muhammad, K., & Waheed, Y. (2023). Nanotechnology: A revolution in modern industry. Molecules, 28(2), 661. https://doi.org/10.3390/molecules28020661

- Martinez, T., Romero, L. S. L., Rodriguez, D. E., & Amaya, J. (2025). A Review for the Design and Optimization of Catalysts: The Use of Statistics as a Powerful Tool for Literature Analysis. Chemistry, 7(3), 74. https://doi.org/10.3390/chemistry7030074

- Mirzaei, M., Zarch, M. B., Darroudi, M., Sayyadi, K., Keshavarz, S. T., Sayyadi, J., Fallah, A., & Maleki, H. (2020). Silica Mesoporous Structures: Effective Nanocarriers in Drug Delivery and Nanocatalysts. Applied Sciences, 10(21), 7533. https://doi.org/10.3390/app10217533:

- Mustapha, S. I., Anekwe, I. M. S., Muritala, K. B., & Isa, Y. M. (2025). Advances in nanocatalysts for biofuel production: Mechanisms, performance, and future perspectives. Materials Today: Sustainability, 32, Article 101246. https://doi.org/10.1016/j.mtsust.2025.101246

- Otandi, N. (2024). Effect of catalyst concentration on reaction rate in organic synthesis in Kenya. Journal of Chemistry, 3(2), 1–11. https://doi.org/10.47672/jchem.2401

- Pramanik, A., Chaudhary, A. A., Sinha, A., Chaubey, K. K., Ashraf, M. S., Basher, N. S., Rudayni, H. A., Dayal, D., & Kumar, S. (2023). Nanocatalyst-based biofuel generation: An update, challenges, and future possibilities. Sustainability, 15(7), 6180. https://doi.org/10.3390/su15076180

- Rodriguez-Sanchez, R., Tres, A., Sala, R., Soler, M. D., Guardiola, F., & Barroeta, A. C. (2021). Effects of free-fatty-acid content and saturation degree of the dietary oil sources on lipid-class content and fatty-acid digestibility along the gastrointestinal tract in broilers from 22 to 37 days of age. Poultry Science, 101(2021), 101261. https://doi.org/10.1016/j.psj.2021.101261:

- Sharma, M., Mahajan, P., Alsubaie, A. S., Khanna, V., Chahal, S., Thakur, A., Yadav, A., Arya, A., Singh, A., & Singh, G. (2024). Next-generation nanomaterials-based biosensors: Real-time biosensing devices for detecting emerging environmental pollutants. Materials Today: Sustainability, 29, 101068. https://doi.org/10.1016/j.mtsust.2024.101068

- Shchegolkov, A. V., Shchegolkov, A. V., Kaminskii, V. V., Iturralde, P., & Chumak, M. A. (2025). Advances in electrically and thermally conductive functional nanocomposites based on carbon nanotubes. Polymers, 17(1), 71. https://doi.org/10.3390/polym17010071.

- Solaymani, S., & Botero, J. (2025). Reducing carbon emissions from transport sector: Experience and policy design considerations. Sustainability, 17(9), 3762. https://doi.org/10.3390/su17093762

- Vijayakumar, G., Thangavel, E., Alshamsi, D., Sherif, M., Murad, A. A., & Sangaraju, S. (2025). A critical review on the prospective role of nanomaterials in the effectual removal of radionuclides from wastewater: State of the art and future challenges. Environmental Technology & Innovation, 41, 104129. https://doi.org/10.1016/j.eti.2025.104129

- Vijayakumar, G., Thangavel, E., Alshamsi, D., Sherif, M., Murad, A. A., & Sangaraju, S. (2025). A critical review on the prospective role of nanomaterials in the effectual removal of radionuclides from wastewater: State of the art and future challenges. Environmental Technology & Innovation, 41, 104129. https://doi.org/10.1016/j.eti.2025.104129

- Wan Osman, W. N. A., Rosli, M. H., Mazli, W. N. A., & Samsuri, S. (2024). Comparative review of biodiesel production and purification. Carbon Capture Science & Technology, 13, Article 100264. https://doi.org/10.1016/j.ccst.2024.100264

- Xie, W., Gao, C., & Li, J. (2021). Sustainable biodiesel production from low-quantity oils utilizing H₆PV₃MoW₈O₄₀ supported on magnetic Fe₃O₄/ZIF-8 composites. Renewable Energy, 168, 927–937. https://doi.org/10.1016/j.renene.2020.12.129.

- Yaghi, M., Chidiac, S., Awad, S., El Rayess, Y., & Zgheib, N. (2025). An overview of biodiesel production via heterogeneous catalysts: Synthesis, current advances, and challenges. Clean Technologies, 7(3), 62. https://doi.org/10.3390/cleantechnol7030062

- Yaghi, M., Chidiac, S., Awad, S., El Rayess, Y., & Zgheib, N. (2025). An overview of biodiesel production via heterogeneous catalysts: Synthesis, current advances, and challenges. Clean Technologies, 7(3), 62. https://doi.org/10.3390/cleantechnol7030062

- Yentekakis, I. V., Gournis, D. P., & Karakassides, M. A. (2023). Nanomaterials in catalysis applications. Catalysts, 13(3), 627. https://doi.org/10.3390/catal13030627: Guan, Z.-L., Wang, Y.-D., Wang, Z., Hong, Y., Liu, S.-L., Luo, H.-W., Liu, X.-L., & Su, B.-L. (2024). The synthesis, characteristics, and application of hierarchical porous materials in carbon dioxide reduction reactions. Catalysts, 14(12), 936. https://doi.org/10.3390/catal14120936

- Chenarani, B., Ghaemi, A., & Hemmati, A. (2025). A comprehensive review on the conversion of CO₂ into solid carbon materials. Carbon Capture Science & Technology, Article 100547. https://doi.org/10.1016/j.ccst.2025.100547

- Zhang, Y., Li, W., Wang, J., Jin, J., Zhang, Y., Cheng, J., & Zhang, Q. (2023). Advancement in utilization of magnetic catalysts for production of sustainable biofuels. Frontiers in Chemistry, 10, 1106426. https://doi.org/10.3389/fchem.2022.1106426