Hybrid Architectures for Topological Quantum Computation: Platform Integration, Device Engineering, and Scalability

Abstract: Hybrid systems have emerged as one of the most promising pathways toward realizing fault-tolerant topological quantum computation. Although topological phases such as fractional quantum hall states and chiral superconductors host non-Abelian anyons capable of supporting protected quantum information, yet, no single physical platform currently satisfies all the requirements for scalable, controllable, and universal quantum computation. Hybrid systems, which are formed by integrating complementary physical ingredients such as superconductivity, strong spin–orbit coupling, magnetic textures, correlated electron states, and engineered lattice geometries, offer an avenue to overcome these limitations. This review provides hybrid engineering strategies that examine topological quantum computation, beginning with foundational principles of topological phases, anyon models, and braiding-based quantum information processing. We then survey major hybrid platforms, including semiconductor–superconductor nanowires, quantum Hall–superconductor interfaces, magnetic–superconductor systems, and Floquet-engineered topological structures. Across these platforms, we analyze mechanisms for realizing non-Abelian quasiparticles, the current state of experimental progress, and the challenges associated with disorder, quasiparticle poisoning, gap protection, and device scalability, while also evaluating a roadmap/framework for comparing the platforms with regard to device and scalability criteria. We also discuss theoretical proposals for achieving universality beyond Majorana zero modes, including parafermions and Fibonacci anyons in hybrid architectures. By mapping the landscape of materials, designs, and physical mechanisms that enable topological quantum computation, this review highlights the key scientific breakthroughs achieved so far and the critical directions required to transform hybrid systems into a practical quantum technology.

Keywords: Topological quantum computation, Hybrid quantum devices, Majorana zero modes, Proximity superconductivity, Quantum Hall–superconductor interfaces, Device scalability, Floquet engineering

# 1. Introduction

Quantum computation offers the potential to solve certain classes of problems more efficiently than classical computing, particularly in areas such as cryptography, quantum simulation, and large-scale optimization. Despite significant progress in developing quantum hardware, most existing qubit platforms remain susceptible to decoherence, operational errors, and environmental noise. These challenges limit the scalability and reliability of current quantum technologies [1-5].

Topological quantum computation (TQC) provides a fundamentally different approach by encoding quantum information in nonlocal degrees of freedom associated with topological phases of matter. In such systems, quasiparticles known as anyons exhibit braiding statistics that can be used to implement quantum gates in a manner intrinsically resistant to local disturbances. When these anyons are non-Abelian, exchanging them performs unitary transformations on a degenerate ground-state subspace which offers a pathway toward naturally fault-tolerant quantum computation [6].

However, the realization of non-Abelian anyons in a scalable and controllable physical platform remains a major scientific challenge. While theoretical models predict that systems such as fractional quantum hall states or chiral superconductors can host non-Abelian excitations, practical limitations which are, extreme experimental conditions, limited tunability, and material disorder which have hindered the construction of large-scale, topologically protected devices [7,8].

This gap between theoretical proposals and experimentally accessible platforms has motivated the exploration of hybrid systems. Hybrid systems combine complementary physical mechanisms, such as superconductivity, spin–orbit coupling, magnetic textures, and strong electron correlations to engineer topological properties that do not naturally occur in any single material. Examples include semiconductor–superconductor heterostructures, quantum Hall–superconductor interfaces, magnetic atom chains on superconductors, and Floquet-driven engineered structures [9,10].

By integrating multiple components into a unified architecture, hybrid systems aim to achieve the essential ingredients of TQC: a gapped topological phase, robust zero-energy modes, tunable parameters, and the capability for qubit initialization, braiding, and readout. Nevertheless, these systems introduce new challenges such as interface disorder, quasiparticle poisoning, soft superconducting gaps, and measurement ambiguities. Understanding the benefits and limitations of hybrid approaches requires a systematic examination of their physical principles, design strategies, and experimental progress [5-9].

This review focuses on the landscape of hybrid systems for topological quantum computation. It analyzes the foundational concepts underlying topological phases, surveys major hybrid platforms developed to date, and evaluates their prospects for scalable quantum technologies. The goal is to provide a comprehensive and accessible overview (see Figure 1) of how hybrid architectures can bridge the gap between theoretical models of non-Abelian anyons and practical implementations capable of supporting fault-tolerant quantum computation.

Figure 1

Overview of hybrid systems for topological quantum computation

# 2. Fundamentals of Topological Quantum Computation

The idea behind topological quantum computation emerges from an observation that certain quantum systems possess global, nonlocal features that cannot be altered by smooth and local perturbations. These features define what are known as topological phases of matter. Unlike conventional phases-such as solids, liquids, or magnets-which are distinguished by symmetry breaking and local order parameters, topological phases are characterized by invariants that remain unchanged unless the system undergoes a phase transition accompanied by the closing of an energy gap. This nonlocal character makes topological phases promising candidates for robust quantum computation, since the encoded information is intrinsically protected from many sources of noise [10-18].

# 2.1 Topological Phases: Concept and Physical Origin

A topological phase is typically a gapped quantum many-body state whose essential properties depend not on microscopic details but on the global topology of the system’s wavefunctions. For example, in two-dimensional electron systems under strong magnetic fields, such as in the quantum Hall effect, the Hall conductance takes quantized values that remain unchanged even when disorder or imperfections are introduced. This remarkable robustness arises from a topological quantity known as the Chern number, which counts how certain geometric phases accumulate across the Brillouin zone. The central idea is that these phases cannot be continuously transformed into trivial phases without closing the bulk energy gap. Closing the gap corresponds to a topological phase transition-meaning a fundamental change in the quantum ground state, not merely a small correction to the system’s properties [12-15].

One of the most important consequences of topology in condensed-matter systems is the bulk-boundary correspondence. This principle states that a nontrivial topology in the bulk necessarily implies the presence of protected surface or boundary states. In the context of superconductors, these boundary states can manifest as Majorana zero modes (MZMs)-localized fermionic excitations whose properties are central to topological quantum computation [12].

2.2 Anyons: Fractional and Non-Abelian Quasiparticles

In three dimensions, particle statistics are limited to bosons and fermions. However, in two dimensions-a key setting for many topological systems-quantum mechanics allows a far richer set of possibilities. Quasiparticles called anyons can exhibit statistics that interpolate between bosonic and fermionic behavior or even act in ways that are altogether new [19].

2.2.1 Abelian anyons

Systems such as fractional quantum Hall states support Abelian anyons whose exchange results in a phase shift. For example, exchanging two quasiparticles in the ν=1/3 Laughlin state introduces a phase of 2π/3. Although Abelian anyons demonstrate the principle of fractional statistics, they do not by themselves provide the computational richness required for topological quantum computation [20].

2.2.2 Non-Abelian anyons and their computational power

More exotic are non-Abelian anyons, which are predicted to exist in certain topological phases such as the Moore-Read state at filling factor ν=5/2 or in topological superconductors hosting Majorana zero modes. Unlike Abelian quasiparticles, non-Abelian anyons do not merely accumulate a phase upon exchange-they transform the state of the system within a degenerate ground-state manifold. Braiding two such anyons performs a unitary operation, meaning the exchange operation itself is a quantum gate.

The simplest example is the Ising anyon, often associated with the presence of Majorana modes. The fusion rule;

σ×σ=1+ψ

means that bringing two Ising anyons together can yield either the vacuum or a fermionic state. This fusion ambiguity is what creates a multi-dimensional Hilbert space capable of encoding quantum information nonlocally.

These statistics make non-Abelian anyons intrinsically fault-tolerant: errors that act locally cannot easily change the global topological state, making decoherence exponentially suppressed under suitable conditions [19, 21].

2.3 Majorana Zero Modes and Topological Superconductivity

Majorana zero modes are the most experimentally accessible realization of non-Abelian anyons. A Majorana mode is a fermionic excitation that is its own antiparticle-mathematically expressed as  γ†=γ. In physical systems, Majorana modes typically arise in topological superconductors, where electron pairing and spin-related interactions combine to produce special mid-gap states localized at edges, vortices, or defects.

2.3.1 The Kitaev chain as a minimal model

A powerful theoretical model for understanding MZMs is the Kitaev chain, a one-dimensional lattice of spinless fermions subject to nearest-neighbor hopping and p-wave superconductivity. The model reveals that, when the chemical potential lies within a certain range relative to the hopping amplitude, the chain enters a topological superconducting phase. In this regime, a pair of Majorana modes appears at the ends of the chain. They represent two halves of a nonlocal fermionic degree of freedom whose occupation encodes quantum information [22-26].

2.3.2 Physical requirements and experimental considerations

In real materials, the topological gap protecting Majorana modes is typically on the order of 0.1-1 meV, depending on the choice of superconductor and the strength of induced pairing. For these modes to remain well-defined, the system must be cooled well below this energy scale-often to temperatures around 10-50 mK. Additionally, the spatial separation of the Majoranas must be larger than the superconducting coherence length to ensure that their wavefunctions do not overlap, as such overlap introduces energy splitting that compromises topological protection. In semiconductor-superconductor nanowires, coherence lengths often range from 100 to 500 nm, motivating device lengths of several microns [22].

2.4 Principles and Requirements for Topological Quantum Computation

For topological qubits to function reliably, several physical conditions must be met, as illustrated in Figure 2, many of which directly influence how hybrid systems are engineered [28].

2.4.1 A robust and sizable energy gap

The system must maintain a bulk energy gap that is significantly larger than the ambient temperature and typical noise scales. The inequality;

kBT≪Δ

ensures that thermal excitations do not lift the ground-state degeneracy or introduce unwanted quasiparticles. This is one reason why many experiments operate at millikelvin temperatures using dilution refrigerators.

2.4.2 Adiabatic braiding and operational timescales

Because braiding operations rely on adiabatic evolution-transporting anyons slowly relative to the system’s energy scales-the time required for braiding must exceed a characteristic threshold set by the inverse of the topological gap. For a typical gap of 0.5 meV, the minimum adiabatic timescale falls in the sub-nanosecond regime. In practice, however, braiding operations are designed to occur over much longer intervals (tens or hundreds of nanoseconds) to fully avoid nonadiabatic transitions [22-24].

2.4.3 Parity conservation and quasiparticle poisoning

The computational basis encoded in Majorana modes depends on fermion parity, a quantity that must remain stable during the computation. Any stray quasiparticle entering the system can flip the parity and corrupt the stored information-a process known as quasiparticle poisoning. Hybrid devices therefore, require materials, interfaces, and geometries that minimize these events and extend the poisoning time far beyond the duration of a braiding operation. Semiconductor-superconductor hybrids have demonstrated poisoning times in the tens of microseconds, which is encouraging but still requires improvement for scalable applications [29, 30].

2.4.4 Spatial separation and coherence

To maintain degeneracy, non-Abelian anyons must remain sufficiently separated so that their wavefunctions do not overlap. In practical systems such as nanowires or quantum Hall edges, this often translates into constraints on device geometry. Wires several micrometers long or quantum Hall regions of similar scale are typical requirements for ensuring that the energy splitting between computational states remains exponentially small.

Figure 2

Key physical requirements for topological quantum computation

3. CATEGORIES OF HYBRID SYSTEMS

Hybrid systems represent one of the most active and promising directions for realizing scalable topological quantum computation. Purely topological materials, while theoretically robust, often require extreme environments or lack tunability for practical applications. Hybrid architectures circumvent these limitations by combining complementary physical effects, such as superconductivity, spin–orbit coupling, magnetic order, and strong electronic correlations, to engineer non-Abelian excitations. By carefully designing these systems, researchers aim to create platforms that host Majorana or parafermionic modes while maintaining coherence and fault tolerance. Across these systems, device performance is influenced by parameters such as induced superconducting gaps, spin–orbit coupling strengths, Zeeman energies, coherence times, and quasiparticle poisoning rates. The following sections describe the major categories of hybrid systems, highlighting their physical principles, experimental signatures, and key parameters.

3.1 Semiconductor-Superconductor Hybrid Systems

Semiconductor nanowires proximitized by conventional superconductors are currently among the most mature and experimentally accessible platforms for Majorana zero modes. Materials such as InSb and InAs provide strong spin-orbit coupling, with Rashba spin-orbit energies typically on the order of 0.1-1 meV, while the proximity effect from epitaxial superconductors such as aluminum or niobium nitride induces a superconducting gap in the wire of approximately 0.1-0.25 meV. An applied magnetic field generates a Zeeman splitting, which must exceed a threshold comparable to the induced gap (often 0.2-0.3 meV for InSb/Al systems) to drive the wire into the topological regime. The resulting Majorana zero modes localize at the wire ends as illustrated in Figure 3, and their coherence depends on the quasiparticle poisoning time, which in high-quality devices can reach microseconds to milliseconds, enabling meaningful gate operations [31]. Experimentally, tunneling spectroscopy reveals zero-bias conductance peaks (ZBCPs) approaching the predicted 2e2/h, while Coulomb blockade experiments demonstrate parity-dependent energy shifts consistent with topological superconductivity. Networks of nanowires, particularly in T-junction geometries, allow the effective braiding of Majorana modes through gate-controlled manipulation of chemical potentials. Realizing coherent braiding in such networks requires uniform wire segments with lengths typically exceeding 1-2 μm, minimal disorder, and ultraclean interfaces to maintain long quasiparticle lifetimes. Despite these technical challenges, semiconductor-superconductor hybrids remain the leading candidate for near-term implementation of topologically protected qubits [31-38].

Figure 3

Semiconductor–superconductor hybrid InSb or InAs  nanowire supporting spatially separated Majorana zero modes

3.2 Quantum Hall-Superconductor Hybrid Systems

Quantum Hall-superconductor hybrids exploit strongly correlated electronic states to create topological order that can host non-Abelian quasiparticles. The fractional quantum Hall state at filling factor ν=5/2 (see Figure 4) is particularly notable for supporting excitations with non-Abelian braiding statistics. Candidate ground states, such as the Pfaffian, anti-Pfaffian, or particle-hole symmetric Pfaffian states, all predict quasiparticles carrying half-integer charge (e/4) and obeying non-Abelian statistics. Coupling the quantum Hall edge to a conventional superconductor induces pairing correlations, leading to hybrid modes that combine superconductivity with non-Abelian properties [39]. Experimental observation requires extreme conditions: magnetic fields of 5-10 T, temperatures below 20 mK, and electron mobilities exceeding 106 cm​2/Vs to reduce disorder and stabilize the fractional state. Interferometric techniques, such as Fabry-Perot and Mach-Zehnder geometries, provide a pathway to detect non-Abelian statistics, although stability and reproducibility are challenged by edge reconstruction and electrostatic fluctuations. Hybridization also allows for controlled quasiparticle tunneling into superconducting contacts, potentially enabling measurement-based operations for topological qubits. While technologically demanding, quantum Hall-superconductor systems demonstrate that strong correlations can be harnessed for robust topological platforms [40-45].

Figure 4

Quantum Hall–superconductor hybrid system at filling factor ν = 5/2. Chiral fractional edge modes hybridize under a superconducting contact, forming non-Abelian quasiparticles (charge e/4) that enable interferometric detection and topological operations

3.3 Magnetic–Superconductor Hybrid Architectures

Magnetic–superconductor hybrids use magnetic atoms or nanostructures on superconducting substrates to engineer localized bound states that can hybridize into topological bands [46]. Linear chains of magnetic atoms, often referred to as Shiba chains, generate in-gap states with energies typically 0.1–1 meV below the superconducting gap. When the chain length exceeds several tens of nanometers and interatomic spacing allows sufficient overlap, these states form topological bands supporting Majorana zero modes at the ends as shown in Figure 5. STM experiments have reported zero-bias peaks localized at chain terminations, consistent with these predictions, though distinguishing them from trivial subgap states caused by inhomogeneities remains critical. Beyond linear chains, engineered magnetic textures or patterned nanomagnets can create synthetic spin–orbit fields, emulating the physics of spin–orbit-coupled nanowires without intrinsic spin–orbit materials. Typical magnetic field strengths used to stabilize these textures are on the order of 0.1–1 T, while superconducting gaps in the underlying substrate range from 0.5–1.5 meV for Pb or Nb. These systems provide exceptional flexibility in designing topological phases, with the potential for atomic-scale control of Majorana modes [46-50].

Figure 5

Magnetic–superconductor hybrid system showing a linear chain of magnetic atoms on a superconducting surface produces hybridized in-gap Shiba states forming a topological band with Majorana zero modes at the chain ends

3.4 Ferromagnet–Spin–Orbit–Superconductor 2D Heterostructures

Two-dimensional hybrid systems integrate superconductivity, spin–orbit coupling, and magnetic order in a planar architecture, enabling multi-mode topological states suitable for scalable qubit arrays. Examples include EuS/Al heterostructures, InAs or InSb quantum wells coupled to superconductors, and Fe-based superconductors with topological surface states [51]. Induced superconducting gaps in these systems typically range from 0.2–0.5 meV, while effective spin–orbit energies can reach 1–5 meV depending on the material and quantum well thickness. Magnetic exchange fields of a few Tesla are often required to drive the system into the topological regime. These 2D heterostructures (see Figure 6) can support multiple spatial modes simultaneously, providing pathways to planar multi-qubit layouts and intra-layer braiding operations. Achieving uniform interfaces, minimizing defects, and controlling chemical composition are critical for maintaining coherence times, which can range from microseconds to milliseconds in optimized devices. When successfully engineered as shown in Figure 6, 2D heterostructures offer a scalable and versatile platform for fault-tolerant topological quantum computation [51-57].

Figure 6

2D ferromagnet–spin–orbit–superconductor heterostructure. A planar semiconductor quantum well combined with a ferromagnetic layer and an overlaid superconducting film supports spin–orbit-coupled topological modes with spatially separated Majorana zero modes (γ)

3.5 Floquet and Dynamically Engineered Hybrid Systems

Floquet engineering employs periodic driving through microwaves, optical fields, or time-dependent gate voltage to induce topological phases in systems that are otherwise trivial. By tuning the driving frequency, amplitude, and polarization, one can generate Floquet Majorana modes, dynamically induce superconducting gaps, and create effective spin–orbit interactions (see Figure 7). Typical driving frequencies range from several GHz to tens of GHz, and amplitudes are selected to balance gap opening with minimal heating [57-58]. These dynamically engineered systems allow for topological properties to be switched on demand, providing exceptional flexibility for quantum control and potentially enabling rapid gate operations. However, maintaining coherence under continuous driving requires careful mitigation of heating and dissipation, with topological lifetimes currently limited to microseconds in most experimental implementations. Despite these challenges, Floquet hybrid systems expand the toolkit for realizing controllable, tunable topological phases that could complement static platforms [57-65].

Figure 7

Floquet-driven hybrid system enabling dynamically controlled topological phases

4. Physical Principles and Design Considerations of Hybrid Topological Platforms

Hybrid topological platforms rely on the careful interplay of superconductivity, spin-orbit coupling, magnetism, and correlated electronic phases to host non-Abelian excitations. Achieving robust topological superconductivity requires a combination of material selection, device engineering, and precise control of experimental parameters [66]. Across all hybrid systems, several universal themes emerge: the induced superconducting gap (Δind), the spin-orbit coupling strength (α), the Zeeman energy (EZ) or exchange field (h), and quasiparticle coherence times (τqp). These parameters dictate whether localized Majorana modes or parafermions can form, remain decoupled, and be manipulated reliably for quantum computation.

The fundamental physical principle underlying hybrid topological systems is the generation of an effective p-wave pairing. In one-dimensional semiconductor nanowires, for instance, the combination of spin-orbit coupling, Zeeman splitting, and s-wave proximity-induced superconductivity produces an effective Hamiltonian:

H=p22m*-μτz+αpσyτz+EZσx+Δindτx,

where p is the momentum along the wire, m* is the effective mass (m*∼0.015me for InSb), μ the chemical potential, α the Rashba spin-orbit coefficient (0.1-5 meV·nm depending on wire diameter and confinement), EZ=gμBB/2 the Zeeman energy, and Δind the induced superconducting gap (0.1-0.25 meV for Al). The Pauli matrices σi and τi act in spin and particle-hole spaces, respectively. The topological phase emerges when:

EZ>Δind2+μ2.

This relation highlights three crucial experimental design parameters: Δind sets the energy scale of topological protection; μ must be tuned within the spin-orbit split bands; and EZ must exceed the critical threshold, which is achieved through external magnetic fields (B∼0.2-0.5 T for InSb, depending on the large g-factor g∼50) [66-73].

4.1 Semiconductor-Superconductor Nanowires

Nanowires provide a highly tunable one-dimensional platform. The topological gap, which defines the energy scale over which Majorana modes are protected, is approximately:

Δtop=ΔindEZEZ2+μ2.

For typical experimental parameters (Δind=0.2 meV, EZ=0.3 meV, μ=0.1 meV), Δtop≈0.15 meV, corresponding to thermal robustness up to T∼1.5 K. Device lengths must exceed twice the coherence length:

ξ=ℏvFΔtop≈200-500 nm,

to prevent hybridization between Majorana modes at opposite ends. Spin-orbit coupling enhances the topological gap and reduces sensitivity to disorder; values of α∼0.2 meV·nm are typical for InAs wires under gating.

Experimental signatures include zero-bias conductance peaks near 2e2/h, hard induced gaps, and parity-dependent energy shifts in Coulomb blockade spectroscopy. However, trivial Andreev bound states can mimic these signatures, motivating careful device engineering and multi-terminal measurement strategies [74-78].

4.1.1 Nanowire Networks and Braiding

Extending from single wires, T-junctions and wire networks allow topological braiding of Majorana modes. The adiabatic braiding condition requires that the braiding time tbraid satisfies:

ℏΔtop≪tbraid≪τqp,

where τqp is the quasiparticle poisoning time, typically microseconds to milliseconds in high-quality devices. Device uniformity, gate fidelity, and long coherence lengths are crucial for successful topological operations [1-4].

4.2 Two-Dimensional Heterostructures

2D semiconductor-superconductor heterostructures extend nanowire concepts to planar geometries, enabling multi-mode topological superconductivity. Examples include InAs or InSb quantum wells proximitized by epitaxial Al layers, as well as Fe-based superconductors like FeTeSe with topological surface states. Typical induced gaps range 0.2-0.5 meV, and spin-orbit energies reach 1-5 meV. Multi-channel architectures allow for intra-layer braiding, offering potential scalability beyond one-dimensional networks.

Key challenges include interface uniformity, defect control, and suppression of subgap states. The topological gap in 2D systems can be approximated by a generalized formula:

Δtop2D=Δind(αkF)2+EZ2(αkF)2+EZ2+μ2,

where kF is the Fermi wavevector of the quantum well. Maintaining Δtop2D≳0.1 meV ensures qubit operation at dilution refrigerator temperatures [6].

4.3 Quantum Hall-Superconductor Systems

Quantum Hall systems exploit strong electronic correlations to host non-Abelian excitations. The ν=5/2 fractional quantum hall state supports Moore-Read Pfaffian or anti-Pfaffian quasiparticles with fractional charge e/4 and non-Abelian braiding statistics. Coupling these states to superconductors induces p-wave pairing along chiral edges, producing Majorana edge modes. Achieving these conditions requires ultra-high mobility samples (μe>106 cm​2/Vs), low temperatures (<20 mK), and strong magnetic fields (5-10 T) [8].

Interferometric devices, such as Fabry-Perot or Mach-Zehnder setups, probe braiding statistics through phase-dependent conductance oscillations. Disorder, edge reconstruction, and electrostatic fluctuations remain significant challenges, but hybrid devices provide a pathway to measurement-based topological operations [6, 15].

4.4 Magnetic Atom Chains and Textures

Magnetic chains deposited on superconductors (Shiba chains) create in-gap states, which overlap to form topological bands hosting Majorana modes at chain ends. Typical Shiba energies lie 0.1-1 meV below the superconducting gap. STM experiments reveal zero-bias peaks, although distinguishing true Majorana states from trivial subgap states requires careful spectroscopy.

Magnetic textures and helical fields provide an alternative approach. By patterning nanomagnets or magnetic films, synthetic spin-orbit interactions emulate nanowire physics, allowing atomic-scale design of topological phases. Exchange fields (h∼1-5 meV) and induced gaps (Δind∼0.5 meV) can be tuned to optimize localization and robustness of Majorana modes [16].

4.5 Floquet and Dynamically Driven Systems

Time-periodic driving enables Floquet engineering, creating topological phases absent in static Hamiltonians. For a driven system with amplitude A and frequency ω, the effective Hamiltonian includes a Floquet-induced gap:

Δeff∼A2ℏω.

Typical drives are in the GHz regime, with amplitudes tuned to open topological gaps of 0.05-0.2 meV while minimizing heating. Floquet systems allow on-demand control of topological phases, but coherence is limited by dissipation and quasiparticle excitation, often restricting operation times to microseconds. Combining Floquet methods with static platforms can provide tunable, dynamically reconfigurable qubits [78, 79].

5. Towards Universal Topological Quantum Computation

Hybrid topological platforms offer promising routes to fault-tolerant quantum information processing, but achieving universal quantum computation requires capabilities beyond the natural scope of the simplest non-Abelian excitations. This section examines the fundamental limitations of Majorana-based systems, explores advanced hybrid strategies to achieve universality, and outlines the fault-tolerance principles and engineering requirements necessary for building scalable topological quantum computers. The discussion integrates physical theory, device engineering, and information-theoretic considerations while highlighting the role of hybridization across materials and quasiparticle types [80].

5.1 Limitations of Majorana-Based Topological Qubits

Majorana zero modes (MZMs) obey Ising anyon statistics, a class of non-Abelian statistics that allows fault-tolerant implementation of only a subset of quantum gates. The braiding of Majoranas implements operations in the Clifford group. Clifford gates include the Hadamard, Pauli gates, and the CNOT (up to measurement and classical feedback). However, the Clifford set alone is insufficient for universal quantum computation [80].

Formally, the gates generated by Majorana braiding correspond to unitary operations of the form:

Uij=expπ4γiγj,

where γi are Majorana operators obeying {γi,γj}=2δij. These operations generate:

U∈Clifford group=⟨H,S,CNOT⟩,

but a universal gate set requires at least one non-Clifford gate, most commonly the T-gate:

T=expiπ8Z.

Because Majorana qubits cannot realize the T-gate through braiding alone, the computational power remains limited to what can be efficiently simulated by classical algorithms. This limitation is deep and structural; it stems from the fusion rules of Ising anyons:

σ×σ=1+ψ,

σ×ψ=σ,  ψ×ψ=1,

which restricts the density of computational states accessible through braiding alone.

Therefore, hybridization is not optional but essential for universality.

Practical Constraints

Even before universality, Majorana systems face experimental constraints:

- Quasiparticle poisoning (typical poisoning times 1-100 μs).

- Finite Majorana overlap due to wire lengths comparable to coherence lengths (L∼500 nm vs. ξ∼200-400 nm).

- Soft superconducting gaps due to disorder or imperfect interfaces (Δsoft/Δhard∼0.2-0.4).

- Environmental noise affecting charging-energy-based systems like Majorana islands.

These limitations motivate the development of hybrid architectures capable of producing richer anyon structures and protected non-Clifford operations.

5.2 Hybrid Strategies for Achieving Universality

5.2.1 Majorana-Parafermion Hybrid Architectures

Parafermions, generalizations of Majoranas with Zn symmetry (typically n=4,6), exhibit more complex fusion rules and support a larger unitary gate set.
They emerge in hybrid systems combining:

- Fractional quantum Hall edges at ν=1/3 or ν=2/3,

- Superconducting proximity coupling, and

- Strong spin-orbit or ferromagnetic interactions.

The topological degeneracy scales as:

dim(H)=nN/2,

significantly richer than Majoranas, which give 2N/2. Parafermionic braiding can produce non-Clifford gates directly.

5.2.2 Fibonacci-Enabling Hybrid Systems

The gold standard for universal topological quantum computation is the Fibonacci anyon, whose braid matrices are dense in SU(2). Several proposals aim to engineer Fibonacci anyons using hybrid systems such as:

Coupled arrays of fractional quantum Hall trenches, Superconductor-quantum spin liquid interfaces, Josephson junction ladders in proximity to chiral topological matter.

Fibonacci anyons obey fusion rules:

τ×τ=1+τ,

and their braiding representation provides universality intrinsically, without magic-state distillation.

5.2.3 Hybrid Majorana-Quantum Dot and Measurement-Based Schemes

Another hybrid path uses Majoranas + quantum dots or Majoranas + Coulomb blockade islands to implement controlled-phase gates that mimic non-Clifford operations. Examples include:

- Landau-Zener transitions through Majorana-dot anticrossings,

- Parity-to-charge conversion enabling projective non-topological rotations,

- Fusion-based computation where measurements-rather than braiding-generate a universal gate set.

A typical controlled-phase operation uses the hybridization Hamiltonian:

H=it(γ1d†+γ2d†-h.c.),

where d is a quantum dot fermion operator. This produces effective phase rotations beyond the Clifford gates [56].

5.3 Fault Tolerance and Error Sources in Hybrid Systems

Topological qubits are intrinsically protected from local noise, but real devices suffer from imperfections that reduce protection.

5.3.1 Quasiparticle Poisoning

Quasiparticles disrupt fermion parity conservation. The poisoning rate:

Γqp=Γ0exp-ΔindkBT,

depends exponentially on the induced gap. Achieving Δind≳200 μeV and keeping T<20 mK is essential.

5.3.2 Disorder and Subgap States

Disorder introduces Andreev bound states that hybridize with Majoranas. The disorder length scale l must satisfy:

l≫ξ=ℏvFΔtop,

ensuring that the topological gap is not fragmented by random potential variations.

Typical requirements:

Nanowire mean free paths >1 μm, Quantum Hall interface roughness < 2 nm, Magnetic atom chains with uniform spacing variation < 3%.

5.3.3 Thermal Noise and Braiding Timescales

To maintain adiabaticity:

tbraid≫ℏΔtop

yet also satisfy:

tbraid≪τqp.

Using typical values (Δtop∼100 μeV), the minimal braid time is ∼5-10 ps, while poisoning times are 1-100 μs. This gives a comfortable operational window but demands precise optical or gate-based timing control [12].

5.3.4 Integration with Error Correction

Hybrid systems will likely operate in conjunction with a higher-level error-correcting code, typically a surface code or color code. The logical error rate satisfies:

pL≈Appth(d+1)/2,

where:

p = physical error rate,

pth∼1% = surface-code threshold,

d = code distance,

A = lattice-dependent constant.

Topological qubits aim for p∼10-6-10-8, drastically reducing required code distances and classical overhead.

6. Experimental Challenges, Engineering Constraints, and Practical Realities of Hybrid Topological Platforms

Hybrid platforms for topological quantum computation combine multiple material classes which include: semiconductors, superconductors, ferromagnets, quantum Hall insulators, and engineered spin textures into a single device architecture. Although conceptually elegant, the practical implementation is enormously challenging. Unlike conventional quantum platforms where one material system dominates, hybrid topological platforms depend critically on the interface between dissimilar materials. The topological phase only emerges when superconductivity, spin–orbit coupling, magnetic fields, electrostatic confinement, and crystalline purity all cooperate simultaneously. Each of these ingredients must fall within a narrow operating window. This section examines, in narrative detail, the dominant obstacles currently limiting the performance, stability, and scalability of hybrid systems [1].

6.1 Disorder, Impurities, and Interfacial Quality

The first and perhaps most fundamental difficulty is disorder. Topological phases require coherent quasiparticle motion over relatively long distances. When materials are brought together, for example, a semiconductor nanowire covered by an epitaxial superconductor, any roughness, contamination, or crystalline mismatch at the interface can scatter electrons and destroy coherence.

Semiconductor nanowires such as InAs and InSb are notoriously sensitive to crystal defects, unintentional doping, surface oxides, and vacancy clusters. Even small amounts of charged impurities at the wire surface cause the local electrostatic potential to fluctuate along its length. This unpredictability makes it difficult to reach the uniform conditions required for a true topological regime. Many experiments have shown that when disorder is significant, zero-energy bound states can appear at wire ends even in the absence of a true topological phase. These “trivial zero modes” often mimic the transport signatures of Majorana modes, causing ambiguity in interpretation.

Interface quality is equally critical. The induced superconducting properties depend on how well the semiconductor couples to the superconductor. If the interface is atomically smooth and chemically bonded as in the case of high-quality Al–InAs heterostructures, the induced superconducting gap is large and hard, meaning few spurious excitations exist within the gap. However, if the interface contains even a thin layer of oxide, contaminants, or lattice defects, the induced superconductivity becomes “soft,” with abundant low-energy states that interfere with topological protection. Achieving perfect interfaces across long wires or extended 2D regions remains one of the hardest fabrication tasks.

6.2 Temperature Constraints and Thermal Excitations

Hybrid systems typically operate at extremely low energy scales. The superconducting gaps involved are often only a few hundred microelectronvolts, which correspond to temperatures of a few tens of millikelvin. Dilution refrigerators can reach such temperatures, but electron temperatures which is the actual temperature experienced by electrons in the device are difficult to push below 30–50 millikelvin.

Even at these temperatures, thermal excitations can generate quasiparticles that interfere with the quantum information stored in Majorana modes. This phenomenon, known as quasiparticle poisoning, happens when thermally activated excitations momentarily enter a superconducting island, change the fermion parity, and disrupt any nonlocal qubit encoded in the system. Experiments often observe poisoning events on microsecond timescales, whereas practical topological qubits require stability over milliseconds or longer.

Another issue is thermal broadening of low-energy conductance features. Because many Majorana detection methods rely on tunneling spectroscopy, thermal smearing at elevated temperatures can blur the zero-bias peaks used to identify topological signatures. This complicates interpretation and makes it harder to distinguish genuine topological states from trivial alternatives [14].

6.3 Magnetic Field Requirements and Superconductor Fragility

Most hybrid systems require an external magnetic field to enter the topological regime. However, superconductors are intrinsically sensitive to magnetic fields, which suppress their superconducting properties. Achieving a balance is therefore extremely delicate: the field must be strong enough to drive the semiconductor into the topological phase, but not so strong that it destroys superconductivity in the parent material.

Thin epitaxial aluminum films have emerged as the most successful superconductors in this regard because they can withstand magnetic fields much stronger than the bulk material. Even so, they remain near their operational limit when pushed into the regimes required for topological transitions. A small misalignment of the magnetic field by even a fraction of a degree can introduce unwanted orbital effects that degrade the superconducting proximity effect.

Magnetic noise also becomes increasingly important at low energies. Fluctuations in the magnetic environment, whether from external sources or from magnetic defects within the device, can shift energy levels and destabilize localized Majorana states. Shielding, filtering, and precise control of magnetic environments are therefore essential, adding further complexity.

6.4 Electrostatic Control, Gate Design, and Device Geometry

Hybrid devices typically incorporate many electrostatic gates that tune the chemical potential, potential barriers, and carrier density in nanowires or 2D materials. These gates must be controlled with extremely high precision. Even slight drifts or fluctuations in gate voltages can push a device out of the topological regime. At millikelvin temperatures, gate voltages can drift over time due to charge rearrangements in the dielectric materials, requiring constant recalibration.

Another challenging issue is cross-capacitance, where adjusting one gate unintentionally affects nearby wires or regions. In simple single-wire experiments this is manageable, but in multi-wire networks such as T-junctions required for braiding, cross-talk becomes a serious obstacle. Scaling the system to even a handful of wires requires complex modeling and iterative tuning, something that becomes exponentially difficult as the number of wires increases.

Device geometry also significantly affects performance. Wire diameter, length, and placement relative to the superconductor change the effective spin–orbit coupling and superconducting proximity effect. Because growth methods cannot perfectly control these dimensions, each device behaves slightly differently, requiring custom tuning. This lack of reproducibility has hindered the transition from small laboratory prototypes to reliable large-scale architectures [1, 15, 80].

6.5 Spurious Bound States, Soft Gaps, and “False Majoranas”

One of the most persistent experimental challenges in the field is the difficulty of distinguishing true Majorana zero modes from trivial states that appear accidentally at zero energy. These trivial states often result from smooth potential variations, disorder-induced localization, or poorly understood subgap features at the semiconductor–superconductor interface. Because they can generate zero-bias peaks similar to those expected from Majoranas, they complicate the interpretation of experiments and sometimes lead to false-positive claims.

A related issue is the soft gap problem, where the density of states inside the induced superconducting gap is non-negligible. A soft gap makes it easier for low-energy excitations to form and interact with localized Majorana states, reducing their robustness. Experiments have gradually improved gap hardness through epitaxial growth techniques, but perfect gap hardness remains difficult to achieve outside of carefully optimized devices.

Subgap states also play a role in quasiparticle poisoning. They act as traps where quasiparticles can reside for long periods before interacting with Majorana modes. Reducing the presence of such traps is crucial but requires exquisite control over material purity and interface quality [12, 80].

6.6 Scaling Challenges: From Single Devices to Large Quantum Architectures

Demonstrating a single Majorana-like feature in a nanowire is significantly easier than constructing a functional quantum computer. Scaling requires dozens or hundreds of wires, braiding junctions, superconducting islands, readout circuitry, and feedback loops. Each additional element introduces new requirements for uniformity, coherence, and control.

One major challenge is device reproducibility. Even on a single chip, nominally identical wires can exhibit different critical fields, chemical potentials, induced gaps, and disorder levels. Large-scale quantum computing requires each qubit to behave nearly identically so that error correction protocols can function. Current fabrication approaches do not consistently achieve such uniformity.

Another scaling bottleneck is the sheer amount of cryogenic wiring required. Each topological qubit demands several electrostatic gates, readout lines, and control signals. Modern dilution refrigerators cannot handle the thermal load from hundreds or thousands of such lines. This creates an engineering limit that must be overcome either through cryogenic multiplexing, new wiring technologies, or entirely new device architectures that reduce per-qubit wiring requirements.

Finally, scaling also amplifies the effects of noise—thermal noise, charge noise, magnetic noise, mechanical vibrations, and telegraph noise—all of which degrade device stability. What is manageable in a small single device becomes debilitating in a large array unless noise sources are reduced by orders of magnitude.

7. Outlook and Future Directions for Scalable Topological Quantum Computing

The field of topological quantum computing is steadily moving from theoretical promise toward experimental realization, yet many scientific and engineering challenges remain before fully scalable architectures can be achieved. One central direction for future progress lies in the continued refinement of qubit materials, particularly the exploration of more robust topological phases capable of surviving disorder, thermal fluctuations, and fabrication imperfections. Although Majorana zero modes remain the most studied platform, emerging candidates such as parafermions, Fibonacci anyons, and intrinsically topological superconducting phases may provide stronger protection and more versatile computational capabilities. The search for these exotic quasiparticles has pushed research deeper into material science, with ongoing efforts focused on designing cleaner heterostructures, optimizing epitaxial interfaces, and improving control over spin–orbit coupling, electron mobility, and induced superconductivity.

Another promising direction concerns the development of hybrid device architectures that combine the strengths of diverse quantum technologies. For instance, coupling topological qubits with high-coherence superconducting qubits may offer a practical route to initialization, measurement, and error mitigation, while integrating them with photonic systems could enable long-distance quantum networking. These hybrid strategies reflect a broader shift toward modular quantum architectures, where topological qubits serve as protected computational cores while conventional qubits act as auxiliary elements for control and communication. Achieving this integration will require advancements in chip-level engineering, interface design, and cryogenic quantum electronics capable of operating at ultralow noise levels.

A long-term objective involves the implementation of fault-tolerant logical operations using topological schemes such as braiding, fusion, and measurement-based control. Although partial demonstrations have been reported, full braiding of non-Abelian anyons in a controlled, programmable setting remains an open milestone. Progress will depend on improved nanofabrication methods that can pattern networks of nanowires and superconducting islands with nanometer-scale precision, as well as more sophisticated measurement protocols capable of resolving subtle topological signatures from background electronic noise. As fabrication becomes more reliable, researchers expect to transition from single-device experiments to the characterization of large arrays containing tens or hundreds of topological modes, opening a realistic pathway to encoding logical qubits and performing small-scale algorithms.

Theoretical research continues to play a vital role in shaping the future landscape, not only by identifying new topological phases but also by proposing efficient error-correction strategies tailored to topologically protected states. While topological qubits are naturally resistant to local noise, they are not completely immune; thus, error processes related to quasiparticle poisoning, residual hybridization, and thermal excitations must be carefully modeled and mitigated. Advancements in simulation methods, topological codes, and noise-aware control protocols will guide experimentalists in building more resilient devices and better understanding the limitations of current approaches.

Finally, achieving scalability will require significant improvements in manufacturing, standardization, and system integration. The field is gradually transitioning from bespoke laboratory devices to reproducible wafer-scale fabrication, supported by collaborations between academia, national laboratories, and semiconductor industries. As these partnerships mature, they are expected to produce the infrastructure necessary for large-scale topological processors, including cryogenic control hardware, ultraclean materials, automated tuning algorithms, and software frameworks capable of orchestrating complex topological operations.

Overall, the future of scalable topological quantum computing rests on a combination of breakthroughs in materials science, device engineering, theoretical modeling, and system-level integration. While substantial challenges remain, the momentum within the field is strong, and each year brings new demonstrations that steadily close the gap between conceptual models and functional quantum processors. If these parallel efforts continue to advance, topological architectures may ultimately provide the stable, fault-tolerant platform required for the next generation of powerful quantum technologies.

# 8. Conclusion

Topological quantum computing represents one of the most promising pathways toward realizing fault-tolerant quantum information processing, offering a fundamentally different strategy from conventional qubit platforms. By encoding information in global topological properties rather than local microscopic degrees of freedom, topological systems provide natural protection against many common decoherence channels. This inherent robustness has motivated extensive research into Majorana zero modes, parafermions, quantum Hall states, and other non-Abelian anyonic platforms, all of which continue to shape the evolving landscape of quantum device engineering. Throughout this review, the discussion has highlighted not only the conceptual foundations of topological phases but also the practical challenges associated with material synthesis, device fabrication, hybrid integration, and scalable control.

Hybrid systems, in particular, are emerging as a pivotal direction for achieving real-world topological quantum processors. By combining the protection offered by topological qubits with the versatility and high-fidelity manipulation available in superconducting, photonic, and semiconductor technologies, hybrid architectures offer a balanced approach that leverages the strengths of multiple quantum platforms. These systems also provide clearer pathways for measurement, state preparation, error mitigation, and reveals areas where purely topological platforms remain technically demanding. As research progresses, the synergy between topological and non-topological components is likely to define the next major breakthroughs in experimental realization.

Despite the remarkable theoretical progress and numerous experimental advancements described in this review, the dream of a large-scale, fully topological quantum computer is still in its developmental stage. Key milestones, such as unambiguous detection of non-Abelian statistics, reliable braiding operations, scalable fabrication of nanowire networks, and robust error-corrected logical qubits, remain active areas of investigation. However, the momentum in the field is accelerating, supported by interdisciplinary collaboration among physicists, materials scientists, electrical engineers, and industry partners. Each incremental achievement contributes to a clearer roadmap for transforming topological concepts into practical quantum technologies.

Looking ahead, the combination of improved material quality, refined theoretical models, advanced cryogenic electronics, and increasingly modular architectures promises to bring topological quantum computing closer to scalable implementation. While the path is challenging, the potential rewards which is a highly stable qubits, reduced overhead for error correction, and long-term architectural scalability make the pursuit both scientifically and technologically compelling. In conclusion, topological quantum computing remains a frontier defined by deep theoretical richness and transformative practical potential, and continued progress across all layers of research will be essential to unlocking its full capabilities.

Disclaimer (Artificial intelligence)

Author(s) hereby declare that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc.) and text-to-image generators have been used during the writing or editing of this manuscript.

# References

Kim, Y., Eddins, A., Anand, S., Wei, K. X., van den Berg, E., Rosenblatt, S., Nayfeh, H., Wu, Y., Zaletel, M., Temme, K., & Kandala, A. (2023). Evidence for the utility of quantum computing before fault tolerance. Nature, 618(7965), 500–505. https://doi.org/10.1038/s41586-023-06096-3

Kandala, A., Temme, K., Córcoles, A. D., Mezzacapo, A., Chow, J. M., & Gambetta, J. M. (2019). Error mitigation extends the computational reach of a noisy quantum processor. Nature, 567(7749), 491–495. https://doi.org/10.1038/s41586-019-1040-7

Siddiqi, I. (2021). Engineering high-coherence superconducting qubits. Nature Reviews. Materials, 6(10), 875–891. https://doi.org/10.1038/s41578-021-00370-4

Hashim, A., Naik, R. K., Morvan, A., Ville, J.-L., Mitchell, B., Kreikebaum, J. M., Davis, M., Smith, E., Iancu, C., O’Brien, K. P., Hincks, I., Wallman, J. J., Emerson, J., & Siddiqi, I. (2021). Randomized compiling for scalable quantum computing on a noisy superconducting quantum processor. Physical Review. X, 11(4). https://doi.org/10.1103/physrevx.11.041039

Cheng, B., Deng, X.-H., Gu, X., He, Y., Hu, G., Huang, P., Li, J., Lin, B.-C., Lu, D., Lu, Y., Qiu, C., Wang, H., Xin, T., Yu, S., Yung, M.-H., Zeng, J., Zhang, S., Zhong, Y., Peng, X., … Yu, D. (2023). Noisy intermediate-scale quantum computers. Frontiers of Physics, 18(2). https://doi.org/10.1007/s11467-022-1249-z

Stilck França, D., & García-Patrón, R. (2021). Limitations of optimization algorithms on noisy quantum devices. Nature Physics, 17(11), 1221–1227. https://doi.org/10.1038/s41567-021-01356-3

Lotem, M., Sela, E., & Goldstein, M. (2022). Manipulating non-abelian anyons in a chiral multichannel Kondo model. Physical Review Letters, 129(22). https://doi.org/10.1103/physrevlett.129.227703

Frolov, S. M., Manfra, M. J., & Sau, J. D. (2020). Topological superconductivity in hybrid devices. Nature Physics, 16(7), 718–724. https://doi.org/10.1038/s41567-020-0925-6

Escribano, S. D., Maiani, A., Leijnse, M., Flensberg, K., Oreg, Y., Levy Yeyati, A., Prada, E., & Seoane Souto, R. (2022). Semiconductor-ferromagnet-superconductor planar heterostructures for 1D topological superconductivity. Npj Quantum Materials, 7(1). https://doi.org/10.1038/s41535-022-00489-9

Chatterjee, P., Ghosh, A. K., Nandy, A. K., & Saha, A. (2024). Second-order topological superconductor via noncollinear magnetic texture. Physical Review. B, 109(4). https://doi.org/10.1103/physrevb.109.l041409

Hart, O., Stephen, D. T., Williamson, D. J., Foss-Feig, M., & Nandkishore, R. (2025). Playing nonlocal games across a topological phase transition on a quantum computer. Physical Review Letters, 134(13). https://doi.org/10.1103/physrevlett.134.130602

Xiao, X., Freericks, J. K., & Kemper, A. F. (2023). Robust measurement of wave function topology on NISQ quantum computers. Quantum, 7(987), 987. https://doi.org/10.22331/q-2023-04-27-987

Azses, D., Haenel, R., Naveh, Y., Raussendorf, R., Sela, E., & Dalla Torre, E. G. (2020). Identification of symmetry-protected topological states on noisy quantum computers. Physical Review Letters, 125(12). https://doi.org/10.1103/physrevlett.125.120502

Smith, A., Jobst, B., Green, A. G., & Pollmann, F. (2022). Crossing a topological phase transition with a quantum computer. Physical Review Research, 4(2). https://doi.org/10.1103/physrevresearch.4.l022020

Shen, R., Chen, T., Yang, B., Zhong, Y., & Lee, C. H. (2025). Robust simulations of many-body symmetry-protected topological phase transitions on a quantum processor. Npj Quantum Information, 11(1). https://doi.org/10.1038/s41534-025-01122-w

Ornelas, P., Nape, I., de Mello Koch, R., & Forbes, A. (2025). Topological rejection of noise by quantum skyrmions. Nature Communications, 16(1), 2934. https://doi.org/10.1038/s41467-025-58232-4

Azizi, F. (2025). Tunable topological phases in 2D materials via nonlocal three-body interactions. Journal of Physics. Condensed Matter: An Institute of Physics Journal, 37(31), 31LT01. https://doi.org/10.1088/1361-648X/adf484

Akanbi, O. S., Shannon, J. P., Delhommelle, J., & Desgranges, C. (2025). Mini Review: Synergizing driven quantum dynamics, AI, and quantum computing for next-gen materials science. The Journal of Physical Chemistry Letters, 16(45), 11821–11832. https://doi.org/10.1021/acs.jpclett.5c02390

Yutushui, M., Hermanns, M., & Mross, D. F. (2025). Non-Abelian phases from the condensation of Abelian anyons. Physical Review Letters, 135(5), 056501. https://doi.org/10.1103/3yvl-4hws

Iulianelli, F., Kim, S., Sussan, J., & Lauda, A. D. (2025). Universal quantum computation using Ising anyons from a non-semisimple topological quantum field theory. Nature Communications, 16(1), 6408. https://doi.org/10.1038/s41467-025-61342-8

Xiao, B., Alvarez, G., & Halász, G. B. (2025). Robustness of vacancy-bound non-Abelian anyons in the Kitaev model in a magnetic field. Physical Review Letters, 135(9), 096603. https://doi.org/10.1103/fl9b-4h4v

Jin, F., Jiang, S., Zhu, X., Bao, Z., Shen, F., Wang, K., Zhu, Z., Xu, S., Song, Z., Chen, J., Tan, Z., Wu, Y., Zhang, C., Gao, Y., Wang, N., Zou, Y., Zhang, A., Li, T., Zhong, J., … Deng, D.-L. (2025). Topological prethermal strong zero modes on superconducting processors. Nature, 645(8081), 626–632. https://doi.org/10.1038/s41586-025-09476-z

Bhowmik, S., & Saha, A. (2025). Topological Majorana zero modes and the superconducting diode effect driven by Fulde-Ferrell-Larkin-Ovchinnikov pairing in a helical Shiba chain. Physical Review. B, 111(16). https://doi.org/10.1103/physrevb.111.l161402

Guo, X., Ma, X., Ying, X., & Law, K. T. (2025). Majorana zero modes in the Lieb-Kitaev model with tunable quantum metric. Physical Review Letters, 135(7), 076601. https://doi.org/10.1103/l3c7-knqm

Cayao, J., & Aguado, R. (2025). Non-Hermitian minimal Kitaev chains. Physical Review. B, 111(20). https://doi.org/10.1103/physrevb.111.205432

Klocke, K., Simm, D., Zhu, G.-Y., Trebst, S., & Buchhold, M. (2025). Entanglement dynamics in monitored Kitaev circuits: Loop models, symmetry classification, and quantum Lifshitz scaling. Physical Review. B, 111(22). https://doi.org/10.1103/physrevb.111.224301

Bauer, A. (2025). x+ y Floquet code: A simple example for topological quantum computation in the path-integral approach. Physical Review A, 111(3).

Giri, M. K., & Mandal, S. B. (2025). Realizing topological quantum walks on NISQ digital quantum computer. Physica Scripta. https://doi.org/10.1088/1402-4896/adb244

Larson, C. P., Yelton, E., Dodge, K., Okubo, K., Batarekh, J., Iaia, V., Kurinsky, N. A., & Plourde, B. L. T. (2025). Quasiparticle poisoning of superconducting qubits with active gamma irradiation. PRX Quantum: A Physical Review Journal, 6(3). https://doi.org/10.1103/2lyd-8swv

Safwan, A. H., & Bomantara, R. W. (2025). Generating non-Clifford gate operations through exact mapping between Majorana fermions and mathbb Z _4  parafermions. Journal of Physics A: Mathematical and Theoretical, 58(33).

Kouwenhoven, L. (2025). Perspective on Majorana bound-states in hybrid superconductor-semiconductor nanowires. Modern Physics Letters. B, Condensed Matter Physics, Statistical Physics, Applied Physics, 39(03). https://doi.org/10.1142/s0217984925400020

Ma, Q., Ai, L., Zhang, Y., & Xiu, F. (2025). Hybrid Superconducting-Magnetic Van der Waals Heterostructures: Physics and Application. Advanced Materials (Deerfield Beach, Fla.), e07866, e07866. https://doi.org/10.1002/adma.202507866

de Moor, M. W. A., Bommer, J. D. S., Xu, D., Winkler, G. W., Antipov, A. E., Bargerbos, A., Wang, G., van Loo, N., Op het Veld, R. L. M., Gazibegovic, S., Car, D., Logan, J. A., Pendharkar, M., Lee, J. S., M Bakkers, E. P. A., Palmstrøm, C. J., Lutchyn, R. M., Kouwenhoven, L. P., & Zhang, H. (2018). Electric field tunable superconductor-semiconductor coupling in Majorana nanowires. New Journal of Physics, 20(10), 103049. https://doi.org/10.1088/1367-2630/aae61d

Lutchyn, R. M., Bakkers, E. P. A. M., Kouwenhoven, L. P., Krogstrup, P., Marcus, C. M., & Oreg, Y. (2018). Majorana zero modes in superconductor–semiconductor heterostructures. Nature Reviews. Materials, 3(5), 52–68. https://doi.org/10.1038/s41578-018-0003-1

Sestoft, J. E., Kanne, T., Gejl, A. N., von Soosten, M., Yodh, J. S., Sherman, D., Tarasinski, B., Wimmer, M., Johnson, E., Deng, M., Nygård, J., Jespersen, T. S., Marcus, C. M., & Krogstrup, P. (2018). Engineering hybrid epitaxial InAsSb/Al nanowires for stronger topological protection. Physical Review Materials, 2(4). https://doi.org/10.1103/physrevmaterials.2.044202

Prada, E., San-Jose, P., de Moor, M. W. A., Geresdi, A., Lee, E. J. H., Klinovaja, J., Loss, D., Nygård, J., Aguado, R., & Kouwenhoven, L. P. (2020). From Andreev to Majorana bound states in hybrid superconductor–semiconductor nanowires. Nature Reviews. Physics, 2(10), 575–594. https://doi.org/10.1038/s42254-020-0228-y

Escribano, S. D., Yeyati, A. L., & Prada, E. (2020). Improved effective equation for the Rashba spin-orbit coupling in semiconductor nanowires. Physical Review Research, 2(3). https://doi.org/10.1103/physrevresearch.2.033264

Kaufhold, L., & Rosch, A. (2025). Stability of Majorana modes in Coulomb-disordered topological insulator nanowires. Physical Review. B, 112(4). https://doi.org/10.1103/bsxt-n9ls

Bonderson, P., Kitaev, A., & Shtengel, K. (2006). Detecting non-abelian statistics in theν=5/2Fractional quantum hall state. Physical Review Letters, 96(1). https://doi.org/10.1103/physrevlett.96.016803

Zhao, L., Arnault, E. G., Larson, T. F. Q., Watanabe, K., Taniguchi, T., Amet, F., & Finkelstein, G. (2024). Nonlocal transport measurements in hybrid quantum Hall–superconducting devices. Physical Review. B, 109(11). https://doi.org/10.1103/physrevb.109.115416

Yutushui, M., & Mross, D. F. (2023). Identifying non-Abelian anyons with upstream noise. Physical Review. B, 108(24). https://doi.org/10.1103/physrevb.108.l241102

Choi, Y., Choi, Y., Valentini, M., Patterson, C. L., Holleis, L. F. W., Sheekey, O. I., Stoyanov, H., Cheng, X., Taniguchi, T., Watanabe, K., & Young, A. F. (2025). Superconductivity and quantized anomalous Hall effect in rhombohedral graphene. Nature, 639(8054), 342–347. https://doi.org/10.1038/s41586-025-08621-y

Willett, R. L. (2013). The quantum Hall effect at 5/2 filling factor. Reports on Progress in Physics. Physical Society (Great Britain), 76(7), 076501. https://doi.org/10.1088/0034-4885/76/7/076501

Kudo, K., Nakai, R., & Nomura, K. (2024). Disorder-induced topological superconductivity in a spherical quantum-Hall–superconductor hybrid. Physical Review. B, 110(3). https://doi.org/10.1103/physrevb.110.035147

Wang, C., Gupta, A., Singh, S. K., Tai, C. T., Pfeiffer, L. N., Baldwin, K. W., Winkler, R., & Shayegan, M. (2025). Even-denominator fractional quantum Hall states with spontaneously broken rotational symmetry. Reports on Progress in Physics. Physical Society (Great Britain), 88(10), 100501. https://doi.org/10.1088/1361-6633/ae0a7f

Schneider, L., Beck, P., Posske, T., Crawford, D., Mascot, E., Rachel, S., Wiesendanger, R., & Wiebe, J. (2021). Topological Shiba bands in artificial spin chains on superconductors. Nature Physics, 17(8), 943–948. https://doi.org/10.1038/s41567-021-01234-y

Rachel, S., & Wiesendanger, R. (2025). Majorana quasiparticles in atomic spin chains on superconductors. Physics Reports, 1099, 1–28. https://doi.org/10.1016/j.physrep.2024.10.005

Wong, K. H., Hirsbrunner, M. R., Gliozzi, J., Malik, A., Bradlyn, B., Hughes, T. L., & Morr, D. K. (2023). Higher order topological superconductivity in magnet-superconductor hybrid systems. Npj Quantum Materials, 8(1). https://doi.org/10.1038/s41535-023-00564-9

Liu, T., Wan, C. Y., Yang, H., Zhao, Y., Xie, B., Zheng, W., Yi, Z., Guan, D., Wang, S., Zheng, H., Liu, C., Fu, L., Liu, J., Li, Y., & Jia, J. (2024). Signatures of hybridization of multiple Majorana zero modes in a vortex. Nature, 633(8028), 71–76. https://doi.org/10.1038/s41586-024-07857-4

Ding, H., Hu, Y., Randeria, M. T., Hoffman, S., Deb, O., Klinovaja, J., Loss, D., & Yazdani, A. (2021). Tuning interactions between spins in a superconductor. Proceedings of the National Academy of Sciences of the United States of America, 118(14). https://doi.org/10.1073/pnas.2024837118

Kezilebieke, S., Huda, M. N., Vaňo, V., Aapro, M., Ganguli, S. C., Silveira, O. J., Głodzik, S., Foster, A. S., Ojanen, T., & Liljeroth, P. (2020). Topological superconductivity in a van der Waals heterostructure. Nature, 588(7838), 424–428. https://doi.org/10.1038/s41586-020-2989-y

González-Ruano, C., Johnsen, L. G., Caso, D., Tiusan, C., Hehn, M., Banerjee, N., Linder, J., & Aliev, F. G. (2020). Superconductivity-induced change in magnetic anisotropy in epitaxial ferromagnet-superconductor hybrids with spin-orbit interaction. Physical Review. B, 102(2). https://doi.org/10.1103/physrevb.102.020405

Hu, J., Yu, F., Luo, A., Pan, X.-H., Zou, J., Liu, X., & Xu, G. (2024). Chiral topological superconductivity in superconductor-obstructed atomic insulator-ferromagnetic insulator heterostructures. Physical Review Letters, 132(3). https://doi.org/10.1103/physrevlett.132.036601

Dizaj, M H. "Quantum Electronics and Its Role in Shaping the Future of Technology." International Conference on Physics.

Dong, Y., Cui, Q., Liao, M., Zhou, H., Xu, T., Qiao, J., Gao, Z., Zhao, M., Chopdekar, R. V., Zhang, D., Yang, H., & Jiang, W. (2024). Possible existence of chiral spin textures in the Bi2Sr2CaCu2O8+δ /Fe1− xTbx heterostructure. Applied Physics Letters, 124(16). https://doi.org/10.1063/5.0200642

Bobkov, G. A., Bobkov, A. M., & Bobkova, I. V. (2024). Spin supercurrent in superconductor/ferromagnet van der Waals heterostructures. Physical Review. B, 110(10). https://doi.org/10.1103/physrevb.110.104506

Liu, B., Zhang, X., Hou, W., Feng, H., Dai, Z., & Guo, Z.-X. (2025). High-performance nonvolatile spin FETs from 2D metallic ferromagnetic and ferroelectric multiferroic heterostructure. Applied Physics Letters, 126(24). https://doi.org/10.1063/5.0267449

Rudner, M. S., & Lindner, N. H. (2020). Band structure engineering and non-equilibrium dynamics in Floquet topological insulators. Nature Reviews. Physics, 2(5), 229–244. https://doi.org/10.1038/s42254-020-0170-z

Yokoyama, T. (2025). Floquet engineering triplet superconductivity in superconductors with spin-orbit coupling or altermagnetism. Physical Review. B, 112(2). https://doi.org/10.1103/4tng-rhc4

Gadge, K., & Manmana, S. R. (2025). Stability of Floquet sidebands and quantum coherence in one-dimensional strongly interacting spinless fermions. Physical Review. B, 112(8). https://doi.org/10.1103/7fzq-zkbv

Wang, D., Ding, Z., Li, M., Tao, Y., & Fu, H. (2024). Explicit-time Floquet topological superconductivity in a microwave/infrared frequency AC voltage-driven Josephson junction. Physical Review Research, 6(2). https://doi.org/10.1103/physrevresearch.6.023059

Acharya, S., Hutchins, A., Akanbi, O., Tang, H., Zhang, Y., Zhang, H., & Guo, W. (2025). Integration of plasmonic nanoheaters for rapid and tunable light‐driven phase transitions in VO₂ nanocomposites. Advanced Materials Interfaces, 12(11). https://doi.org/10.1002/admi.202500035

Gao, M.-J., Ma, Y.-P., & An, J.-H. (2024). Majorana modes and their Floquet engineering in a trapped-ion system. Physical Review. B, 109(18). https://doi.org/10.1103/physrevb.109.184518

Huang, R., Cai, Q.-Y., Nosrati, F., Lo Franco, R., & Man, Z.-X. (2025). Steady-state coherence in multipartite quantum systems: its connection with thermodynamic quantities and impact on quantum thermal machines. Quantum Science and Technology, 10(3), 035001. https://doi.org/10.1088/2058-9565/adcae5

Ito, S., Schüler, M., Meierhofer, M., Schlauderer, S., Freudenstein, J., Reimann, J., Afanasiev, D., Kokh, K. A., Tereshchenko, O. E., Güdde, J., Sentef, M. A., Höfer, U., & Huber, R. (2023). Build-up and dephasing of Floquet-Bloch bands on subcycle timescales. Nature, 616(7958), 696–701. https://doi.org/10.1038/s41586-023-05850-x

Flensberg, K., von Oppen, F., & Stern, A. (2021). Engineered platforms for topological superconductivity and Majorana zero modes. Nature Reviews. Materials, 6(10), 944–958. https://doi.org/10.1038/s41578-021-00336-6

Schirmer, J., Jain, J. K., & Liu, C.-X. (2024). Topological superconductivity induced by spin-orbit coupling, perpendicular magnetic field, and superlattice potential. Physical Review. B, 109(13). https://doi.org/10.1103/physrevb.109.134518

Roy, B. B., Jaiswal, R., Stanescu, T. D., & Tewari, S. (2024). Stabilizing topological superconductivity in disordered spin-orbit coupled semiconductor-superconductor heterostructures. Physical Review. B, 110(11). https://doi.org/10.1103/physrevb.110.115436

Wang, G., Dvir, T., Mazur, G. P., Liu, C.-X., van Loo, N., Ten Haaf, S. L. D., Bordin, A., Gazibegovic, S., Badawy, G., Bakkers, E. P. A. M., Wimmer, M., & Kouwenhoven, L. P. (2022). Singlet and triplet Cooper pair splitting in hybrid superconducting nanowires. Nature, 612(7940), 448–453. https://doi.org/10.1038/s41586-022-05352-2

Chen, J., Yu, P., Stenger, J., Hocevar, M., Car, D., Plissard, S. R., Bakkers, E. P. A. M., Stanescu, T. D., & Frolov, S. M. (2017). Experimental phase diagram of zero-bias conductance peaks in superconductor/semiconductor nanowire devices. Science Advances, 3(9), e1701476. https://doi.org/10.1126/sciadv.1701476

Hutchins, A., Acharya, S., Akanbi, O., Doan, K., Pinninti, P., Isherwood, K., Rosenberg, Z., Filocamo, S., Zhang, Y., & Guo, W. (2025). Low-power textile-integrated electroosmosis pump for active moisture and sweat management. iScience, 28(12), 114165. https://doi.org/10.1016/j.isci.2025.114165

Khindanov, A., Alicea, J., Lee, P., Cole, W. S., & Antipov, A. E. (2021). Topological superconductivity in nanowires proximate to a diffusive superconductor–magnetic-insulator bilayer. Physical Review. B, 103(13). https://doi.org/10.1103/physrevb.103.134506

Das Sarma, S., Sau, J. D., & Stanescu, T. D. (2023). Spectral properties, topological patches, and effective phase diagrams of finite disordered Majorana nanowires. Physical Review. B, 108(8). https://doi.org/10.1103/physrevb.108.085416

Puglia, D., Martinez, E. A., Ménard, G. C., Pöschl, A., Gronin, S., Gardner, G. C., Kallaher, R., Manfra, M. J., Marcus, C. M., Higginbotham, A. P., & Casparis, L. (2021). Closing of the induced gap in a hybrid superconductor-semiconductor nanowire. Physical Review. B, 103(23). https://doi.org/10.1103/physrevb.103.235201

Valentini, M., Borovkov, M., Prada, E., Martí-Sánchez, S., Botifoll, M., Hofmann, A., Arbiol, J., Aguado, R., San-Jose, P., & Katsaros, G. (2022). Majorana-like Coulomb spectroscopy in the absence of zero-bias peaks. Nature, 612(7940), 442–447. https://doi.org/10.1038/s41586-022-05382-w

Awoga, O. A., Cayao, J., & Black-Schaffer, A. M. (2022). Robust topological superconductivity in weakly coupled nanowire-superconductor hybrid structures. Physical Review. B, 105(14). https://doi.org/10.1103/physrevb.105.144509

Hutchins, A., Reens, D., Kharas, D., West, G.N., Sorace-Agaskar, C., Chiaverini, J., McConnell, R., Swint, R., Akanbi, O., Harding, S. and Guo, W., 2024. Fiber-to-Chip Packaging With Robust Fiber Fusion Splicing for Low-Temperature Applications. IEEE Photonics Technology Letters, 36(19), pp.1209-1212. https://doi.org/10.1109/LPT.2024.3452039

Kousar, B., Carrad, D. J., Stampfer, L., Krogstrup, P., Nygård, J., & Jespersen, T. S. (2022). InAs/MoRe hybrid semiconductor/superconductor nanowire devices. Nano Letters, 22(22), 8845–8851. https://doi.org/10.1021/acs.nanolett.2c02532

Bukov, M., D’Alessio, L., & Polkovnikov, A. (2015). Universal high-frequency behavior of periodically driven systems: from dynamical stabilization to Floquet engineering. Advances in Physics, 64(2), 139–226. https://doi.org/10.1080/00018732.2015.1055918

Freedman, M., Nayak, C., & Walker, K. (2006). Towards universal topological quantum computation in the ν= 5 2 fractional quantum Hall state. Physical Review B-Condensed Matter and Materials Physics, 73(24).

- .