SORPTION OF METHYLENE BLUE FROM AQUEOUS SOLUTION USING CARBON AND CHEMICALLY MODIFIED CARBON FROM PERIWINKLE SHELL

ABSTRACT

Carbonized periwinkle shell was modified by two types of activation: alkaline modification with 1 M NaOH and acidic modification with 1 M HNO3. The three carbon samples thus produced were tested for the removal of methylene blue from solution. This test was carried out to provide a cheap and readily available dosage. Chemical treatment of the sample was aimed at increasing surface functional groups. The alkaline modified sample introduced more hydroxyl group to the sample, while the acid modified produced less OH group. The amount of adsorbate removed was shown to be pH dependent with the three samples performing best at higher pH values of 9. Optimum adsorption was achieved at an adsorbent dose of 2g. The isotherm data obeyed the Langmuir model and first order kinetics. The maximum removal of dye at 2g of adsorbent dosage for 2hrs was 56.8%ss for the alkaline modified, 48.0% for the unmodified and 34.4% for the acid modified samples.

Keywords: adsorbate, dosage, isotherm, Langmuir, methylene

- INTRODUCTION

The Federal Government of Nigeria has a new policy of encouraging local industries in the manufacture of products within the country instead of importation. In this regard a ban was imposed on the importation of some products. Chief amongst them is textile product. The policy is geared into strengthening the local economy, but inevitably as with many industrial activities pollution becomes a significant factor. Many industries use dyes and pigments to colour their products, a number of these becomes constituents of the industries waste; which could be hazardous to the environment if not adequately managed [1].

Textile and refining industries produce effluents of wide varieties, amongst which are various inorganic compounds, polymers and heavy metals such as Cr, Ni, Cu these chemical substances are present in textile effluents as coloured compounds, dissolved or suspended solids. Since decolorization of textile effluents does not occur when treated aerobically by municipal sewage systems, adsorption on solid surfaces incorporated to such systems will improve the efficiency of treatment [2]. Among the dye classification, the basic and diazo direct dyes are known to have the highest rates of toxicity (LD50 values are found to be greater than 2 X 1023 mg/kg). The removal of basic dyes such as methylene blue by adsorption by low cost adsorbents have been studied by many researchers [3], [4].

2.0 MATERIAL AND METHOD

2.1 ACID AND ALKALINE MODIFICATION

The dried activated carbon was soaked in a beaker with 1M dilute nitric acid solution. The oxidation was carried out for 24 hrs. the oxidized carbon was washed with distilled water to remove residual acid and was sun dried for 4 hrs. the same method was used for alkaline activation using 1M solution of sodium hydroxide.

2.2 DETERMINATION OF SURFACE FUNCTIONAL GROUP BY INFRARED

The spectra of the carbon samples were recorded using KBr disc in conjunction with a Pekin-Elmer infrared spectrophotometer. KBr disc were prepared by mixing a given sample of KBr crystals, the resulting mixture being ground to a fine powder and heated for 1 hr at 373K. Finally, the mixture was pressed into a KBr disc under vacuum conditions and used as such for IR studies.

2.3 CALIBRATION EXPERIMENT

Concentration of 0ppm, 2ppm, 4ppm, 8ppm, 10ppm were prepared from the stock solution. The absorbencies were taken without adding the carbon, absorbance was taken at 665 nm.

2.4 POINT ZERO CHARGE

50ml 0.01M sodium chloride was placed in a closed flask. The pH was adjusted to values of 4.64, 6, 6.33, 8.00, 10 and 11.80 by adding 0.1M hydrogen chloride or 0.1M sodium hydroxide solutions. Then 0.15g of each sample was added to 50ml at each pH and the final pH taken after 48hrs under agitation at room temperature. (150rpm)

2.5 EFFECTS OF ADSORBENT DOSE ON METHYLENE BLUE UPTAKE FROM SOLUTION

A concentration of 100mg/dm3 was prepared from the stock solution. Masses of 0.5, 1, 1.5, and 2g of the carbon were added to 25ml of the solution. The solutions were agitated for 6hrs at 150rpm with the absorbances taken thereafter.

2.6 EFFECT OF PH ON METHYLENE BLUE UPTAKE FROM SOLUTION

A concentration of 100mg/dm3 was prepared from the stock solution. A constant mass of 2g was added to 25ml of the solution at pH of 3, 4, 5, 7 and 9. The samples were agitated for 6hrs at 150rpm with the absorbencies taken thereafter, pH corrections was done using dilute HCl and NaOH

2.7 EFFECT OF INITIAL CONCENTRATION ON ADSORPTION KINETICS

2g of each sample was added to 100ml concentration of 100mg/dm3, at pH 7 and stirred with a magnetic stirrer, 5ml was withdrawn with syringe at intervals of 0, 30, 60, 90, 120mins respectively. Their various absorbencies were then taken.

2.8 ADSORPTION ISOTHERM

Adsorption isotherm was carried out at concentrations of 100mg/dm3. 2g of each sample was put into 25ml of each concentration. It was then shaken briefly and allowed to stand for two days after which the solution is filtered and absorbance taken.

3.0 RESULT AND DISCUSSION

3.1 DETERMINATION OF SURFACE ACIDIC GROUPS BY INFRARED SPECTROSCOPY

Untreated Carbon

The spectrograph shows a strong and broad peak at 3444.7cm-1, which is the –OH stretch of alcohol, the strong peak at 1680.1cm-1 corresponds to the C=O stretch of conjugated carbonyl compound the medium peak at 2745.3cm-1 is the C-H stretch of aldehyde and the sharp peak at 2876.6cm-1 is the C-H stretch of alkane the medium peak at 1427.2cm-1 is the bending of the methyl group

Modified carbon; alkaline modification

The spectrograph shows a strong and broad peak at 3460cm-1 typical of hydrogen bonded OH stretch and the medium and sharp peak at 3638.7cm-1 indicates the presence -OH functional group. The medium band at 2513.3cm-1 represents C-H stretch of aldehyde and the peak at 1804.8cm-1 represents C = O stretch of aldehydes. The peak at 1644.1cm-1 is the C = C stretch of alkenes.

Modified carbon; acid modification

There was minimal increase in sensitivity of the -OH group as compared to that of alkaline activation. The band at 1694.6cm-1 is a C = O stretch which corresponds to the wavelength of absorbance of amide group RCONH2

3.2 POINT ZERO CHARGE

Experimental results of the pHpzc (pH of the point zero charge) determination are illustrated in table 3.1 below. They are given as the pH values of filtered solutions after equilibrium (pHf) of solution. Taking values from where they cut the x-axis which is their point of electro-neutrality it is shown that the pHpzc of the unmodified carbon, alkaline modified carbon and HNO3 modified carbon were 8.88, 8.91 and 8.83 respectively.

POINT ZERO CHARGE AT 100mg/dm3

Table 3.1 Unmodified activated carbon

| Initial pH | Final pH | Change in pH |
| --- | --- | --- |
| 4.64 | 8.62 | 4.00 |
| 6.00 | 8.71 | 2.75 |
| 6.33 | 8.83 | 2.44 |
| 8.00 | 8.87 | 0.85 |
| 10.00 | 8.96 | -1.05 |
| 11.80 | 9.44 | -2.4 |

Table 3.2 Modified alkaline activated carbon

| Initial pH | Final pH | Change in pH |
| --- | --- | --- |
| 4.64 | 8.64 | 3.98 |
| 6.00 | 8.74 | 2.71 |
| 6.33 | 8.77 | 2.50 |
| 8.00 | 8.85 | 0.87 |
| 10.00 | 8.95 | -1.04 |
| 11.80 | 9.40 | -2.36 |

Table 3.3 HNO3 modified activated carbon

| Initial pH | Final pH | Change in pH |
| --- | --- | --- |
| 4.64 | 8.42 | 3.78 |
| 6.00 | 8.56 | 2.56 |
| 6.33 | 8.65 | 2.32 |
| 8.00 | 8.74 | 0.74 |
| 10.00 | 8.95 | -1.05 |
| 11.80 | 9.59 | -2.21 |

3.3 EFFECT OF SORBENT DOSE ON THE SORPTION OF METHYLENE BLUE UNTO ACTIVATED CARBON WITH 100mg/dm3 AQUEOUS SOLUTION OF METHYLENE BLUE

The effect of absorbent mass on the rate of uptake was studied with other conditions remaining constant with concentration of 100mg/dm3 of the aqueous solution of methylene blue shows a decrease in absorbance, from 0.5g – 2g in table 3.4 – 3.6 for each carbon sample indicating an increase in the removal of methylene blue from aqueous solutions with increase in adsorbent mass due to presence of more site for adsorption as the mass increase.

Comparison between the three samples shows that the alkaline modified activated carbon shows a better adsorption as compared to that of the unmodified and acidic adsorbent. This could be due to increase of negative charges on the surface of the adsorbent. for the alkaline modified activated carbon 2g of activated carbon showed a better performance as compared to others.

Table 3.4 Effect of Aqueous NaOH modified carbon with percentage dye removed

| Mass(g) | Absorbance | Equilibrium conc (mg/dm3) | Amount adsorbed (mg/g) | % Dye removed |
| --- | --- | --- | --- | --- |
| 0.50 | 6.96 | 55.20 | 2.24 | 44.8 |
| 1.00 | 6.40 | 50.80 | 1.23 | 49.2 |
| 1.50 | 5.72 | 45.40 | 0.91 | 54.6 |
| 2.00 | 5.44 | 43.20 | 0.71 | 56.8 |

Table 3.5 Effect of HNO3 activated adsorbent dosage on percentage dye removed

| Mass(g) | Absorbance | Equilibrium conc (mg/dm3) | Amount adsorbed (mg/g) | % Dye removed |
| --- | --- | --- | --- | --- |
| 0.50 | 0.24 | 61.40 | 1.93 | 38.60 |
| 1.00 | 0.12 | 60.80 | 0.98 | 39.20 |
| 1.50 | 0.10 | 55.20 | 0.78 | 46.80 |
| 2,00 | 0.08 | 52.00 | 0.60 | 48.00 |

Table 3.6 Effect of unmodified adsorbent dosage on percentage dye removed

| Mass(g) | Absorbance | Equilibrium conc (mg/dm3) | Amount adsorbed (mg/g) | % Dye removed |
| --- | --- | --- | --- | --- |
| 0.50 | 0.21 | 67.20 | 1.64 | 32.80 |
| 1.00 | 0.11 | 66.40 | 0.84 | 33.60 |
| 1.50 | 0.07 | 66.40 | 0.56 | 33.60 |
| 2.00 | 0.05 | 65.60 | 0.43 | 34.40 |

3.4 EFFECT OF pH ON SORPTION OF METHYLENE BLUE UNTO ACTIVATED CARBON AT 100mg/dm3

The pH value of the solution was an important controlling parameter in the adsorption process, and the initial pH value of the solution has more influence than the final pH. The amount of methylene blue absorbed at 100mg/dm3 initial concentration was minimum at initial pH 3, then increased and remained nearly constant over the initial pH range from 7 – 9. The amount of methylene blue adsorbed was not seriously altered from pH 7 – 9. Hence pH 7 was chosen for study of contact time. The amount of dye adsorbed on the carbon samples as a function of 100mg/dm3 of dye addition is shown in tables 3.7 – 3.9. there was a sharp increase in amount adsorbed for the alkaline treated carbon as compared with the others from pH 3 – 6. The other samples did not show such sharp increase although adsorption increased. This result thus shows that pH is essential in providing favourable adsorbent surface change for adsorption to occur. As the pH of a dye solution increase, the association of dye cations with more negatively charged carbon could more easily take place.

EFFECT OF pH ON SORPTION OF METHYLENE BLUE

Table 3.7 Effect of pH on methylene blue adsorption by using (2g) of alkaline modified carbon

| pH | Absorbance | Equilibrium conc. (mg/dm3) | Amount adsorbed (mg/g) | % Dye removed |
| --- | --- | --- | --- | --- |
| 3 | 10.99 | 87.20 | 0.16 | 12.80 |
| 4 | 6.40 | 56.80 | 0.54 | 43.20 |
| 6 | 2.11 | 16.84 | 1.04 | 83.20 |
| 7 | 1.31 | 10.40 | 1.12 | 89.60 |
| 9 | 1.31 | 10.40 | 1.12 | 89.60 |

Table 3.8 Effect of pH on methylene blue adsorption by using (2g) of HNO3 modified carbon

| pH | Absorbance | Equivalent conc. (mg/dm3) | Amount adsorbed (mg/g) | % Dye removed |
| --- | --- | --- | --- | --- |
| 3 | 12.50 | 99.20 | 0.01 | 0.80 |
| 4 | 11.49 | 91.20 | 0.11 | 8.80 |
| 6 | 9.48 | 75.20 | 0.31 | 24.80 |
| 7 | 8.47 | 67.20 | 0.41 | 32.80 |
| 9 | 7.96 | 63.20 | 0.46 | 36.80 |

Table 3.9 Effect of pH on methylene blue adsorption by using (2g) of unmodified carbon

| pH | Absorbance | Equivalent conc. (mg/dm3) | Amount adsorbed (mg/g) | % Dye removed |
| --- | --- | --- | --- | --- |
| 3 | 12.30 | 97.60 | 0.03 | 2.40 |
| 4 | 10.53 | 85.60 | 0.18 | 14.40 |
| 6 | 7.36 | 58.40 | 0.52 | 41.60 |
| 7 | 6.45 | 51.20 | 0.61 | 48.20 |
| 9 | 6.05 | 48.00 | 0.65 | 52.00 |

3.5 EFFECT OF CONTACT TIME

It can be observed from table 3.10 – 3.15 that uptake increased with time and at some point in time reached an almost constant value where no more dye is removed from the solution. At this point, the amount of dye being adsorbed onto the adsorbent is in a state of dynamic equilibrium with the amount of dye desorbed from the adsorbent. The time required to attain this state of equilibrium was termed the equilibrium time and the amount of dye adsorbed at the equilibrium time reflected the equilibrium dye adsorption capacity of adsorbent under these particular conditions. The result showed that the equilibrium states were attained at 210mins.  for the alkaline treated carbon, 210mins, for the acid treated and 210mins for the untreated samples respectively. The maximum amount of dyes adsorbed at the different times were 1.20, 0.79, 1.09mg/g respectively. The study showed that treatment of the activated carbon had no effect on the time to reach equilibrium.

Table 3.10 Effect of contact time on methylene blue adsorption at 100mg/dm3 for alkaline modified carbon

| Time (mins) | Absorbance | Equilibrium conc. (mg/dm3) | Amount adsorbed (mg/g) | % Dye removed |
| --- | --- | --- | --- | --- |
| 0 | 0 | 0 | 0 | 0 |
| 30 | 5.54 | 44.00 | 0.70 | 56.00 |
| 60 | 3.23 | 25.60 | 0.93 | 74.40 |
| 90 | 2.12 | 16.80 | 1.04 | 83.20 |
| 120 | 1.51 | 12.00 | 1.10 | 88.00 |
| 150 | 0.91 | 7.20 | 1.16 | 92.80 |
| 180 | 0.61 | 4.80 | 1.19 | 95.20 |
| 210 | 0.50 | 4.00 | 1.20 | 96.00 |
| 240 | 0.30 | 2.40 | 1.22 | 97.60 |
| 270 | 0.20 | 1.60 | 1.23 | 98.40 |
| 300 | 0.20 | 1.60 | 1.23 | 98.40 |

Table 3.11 Effect of contact time on methylene blue adsorption at 100mg/dm3 for HNO3 modified carbon

| Time (mins) | Absorbance | Equilibrium conc. (mg/dm3) | Amount adsorbed (mg/g) | % Dye removed |
| --- | --- | --- | --- | --- |
| 0 | 0 | 0 | 0 | 0 |
| 30 | 10.28 | 81.60 | 0.23 | 18.40 |
| 60 | 7.76 | 1.60 | 0.48 | 38.40 |
| 90 | 6.45 | 51.20 | 0.01 | 48.80 |
| 120 | 5.65 | 44.80 | 0.69 | 55.20 |
| 150 | 5.04 | 40.00 | 0.75 | 60.00 |
| 180 | 4.84 | 30.40 | 0.77 | 1.60 |
| 210 | 6.64 | 36.80 | 0.79 | 63.20 |
| 240 | 4.54 | 36.00 | 0.80 | 64.00 |
| 270 | 4.44 | 35.20 | 0.81 | 64.80 |
| 300 | 4.33 | 34.40 | 0.82 | 65.60 |

Table 3.12 Effect of contact time on methylene blue adsorption at 100mg/dm3 for unmodified carbon

| Time (mins) | Absorbance | Equilibrium conc. (mg/dm3) | Amount adsorbed (mg/g) | % Dye removed |
| --- | --- | --- | --- | --- |
| 0 | 0 | 0 | 0 | 0 |
| 30 | 7.36 | 58.4 | 0.52 | 41.60 |
| 60 | 4.13 | 32.80 | 0.84 | 67.20 |
| 90 | 2.62 | 20.80 | 0.99 | 79.20 |
| 120 | 1.36 | 16.80 | 1.04 | 83.20 |
| 150 | 1.81 | 14.40 | 1.07 | 85.60 |
| 180 | 1.71 | 13.60 | 1.08 | 86.40 |
| 210 | 1.61 | 12.8 | 1.09 | 87.20 |
| 240 | 1.51 | 12.0 | 1.10 | 88.00 |
| 270 | 1.41 | 11.2 | 1.11 | 88.80 |
| 300 | 1.31 | 10.4 | 1.12 | 89.60 |

Table 3.13 Equilibrium study of NaOH modified carbon at 100mg/dm3 concentration of methylene blue

| Time (mins) | Equivalent conc. (mg/dm3) (x) | Log (a - x) |
| --- | --- | --- |
| 0 | 0 | 0 |
| 30 | 19.05 | 1.9082 |
| 60 | 16.52 | 1.9216 |
| 90 | 12.88 | 1.9401 |
| 120 | 9.95 | 1.9545 |
| 150 | 7.20 | 1.9675 |
| 180 | 4.80 | 1.9786 |
| 210 | 2.43 | 1.9893 |
| 240 | 2.40 | 1.9985 |

Table 3.14 Equilibrium study of unmodified carbon at 100mg/dm3 concentration of methylene blue

| Time (mins) | Equivalent conc. (mg/dm3) (x) | Log (a - x) |
| --- | --- | --- |
| 0 | 0 | 0 |
| 30 | 20.37 | 1.8991 |
| 60 | 19.20 | 1.9074 |
| 90 | 17.24 | 1.9169 |
| 120 | 16.23 | 1.9231 |
| 150 | 14.79 | 1.9305 |
| 180 | 13.60 | 1.9365 |
| 210 | 12.60 | 1.9415 |
| 240 | 11.61 | 1.9464 |

Table 3.15 Kinetics of acid modified carbon at 100mg/dm3 concentration of methylene blue

| Time (mins) | Equivalent conc. (mg/dm3) (x) | Log (a - x) |
| --- | --- | --- |
| 0 | 0 | 0 |
| 30 | 60.66 | 1.5948 |
| 60 | 56.92 | 1.6343 |
| 90 | 51.20 | 1.6884 |
| 120 | 44.80 | 1.7419 |
| 150 | 40.00 | 1.7782 |
| 180 | 36.96 | 1.7996 |
| 210 | 32.28 | 1.8307 |
| 240 | 26.51 | 1.8662 |

3.6 EQUILIBRIUM STUDY

The analysis of the isotherm data is important to develop an equation, which accurately represents the results and could be used for the design purpose. In order to investigate the sorption isotherm, two models were analyzed: the Langmuir and the Freundlich [31], the Langmuir is perhaps the best known of all the isotherms describing sorption. The theoretical Langmuir isotherm is often used to describe sorption of a solute from a liquid solution as:

qc=qm ka ca1+kaCc    ……………………………………………………………………………………………………2.8

The constants qm and ka are the characteristics of the Langmuir equation and can be determined from a linearized form of equation 2.8 represented by.

Ccqc= 1qmka+Ccqm

Where Cc is the equilibrium concentration (mg/dm3); qc the amount of methylene blue sorbed (mg/g), ka is sorption equilibrium constant (dm3/mg)

CONCLUSION

The activated carbon from periwinkle shell showed appreciable sensitivity towards modification especially for the alkaline modification. There was a slight increase in the amount of surface charge as a result of chemical treatment. Despite this fact, the unmodified sample performed better due to low positive charges on the surface as compared to that of acid activated sample.

The peaks in the spectrograph showed the presence of alkyl. Aldehyde, hydroxyl groups. There was increase in percentage removal with increase in sorbent dose due to more reactive sites but a decrease in amount absorbed per unit mass. The adsorption was pH dependent with adsorption increasing with increase in pH for the three samples. The kinetics and isotherm fitted well into both first-order kinetics and their Langmuir isotherm respectively.

From the observation, it is seen that carbonized periwinkle shell, modified or unmodified produce a significant removal of methylene blue from aqueous solution, hence it can serve as a good, cheap and readily available alternative for adsorbing dyes from textile effluents.

Disclaimer (Artificial intelligence)

Option 1:

Author(s) hereby declare that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc.) and text-to-image generators have been used during the writing or editing of this manuscript.

Option 2:

Author(s) hereby declare that generative AI technologies such as Large Language Models, etc. have been used during the writing or editing of manuscripts. This explanation will include the name, version, model, and source of the generative AI technology and as well as all input prompts provided to the generative AI technology

Details of the AI usage are given below:

1.

2.

3.

REFERENCE

- Uluatam J., (1991) Am. Water Works Association. 70 – 71

- Anliker R., (1979) Ecotoxicology of dye – stuffs. Ecotox. Environ. Safe 3, 2.

doi: 10.1016/0147-6513(79)90060-5

- Rahman I.A and Saad B (2003) Malaysian Journal of Chemistry Vol.5 1008 – 1014

- Low K.S., Lee C.K. and Tan K.K. (1995) Bioresource Technology Issue 52 : 79 – 83

doi: 10.1016/0960-8524(95)00007-2

- Glover B and Hill L (1993) Tex. Chem. Col. 25(6):15

- Troxler R.W and Hopkins K.S (1982) Roc. 30th Ind-Waste Conference. Ann Arbor Science: 755

- Guiza S. (2004) Adsorption of basic-dyes on natural clay. Bioresource Technology Issue 17: 245

https://doi.org/10.1016/S0043-1354(01)00056-2

- Diaper C., Corresa V.M. and Judd S.J. (1996) JSDC Vol. 112: 273

- Erswell A., Brouckaen C.J. and Backley C.A. (1988) Desalination Vol. 70:157

- Porter J.J (1990) Amer. Dye Stuff Report Vol.22(6):21

- Sloker Y.M. and Le Marechal A.M. (1997) Methods of decolouration of textile wastewaters. Dyes Pigment Vol.37: 335 – 336

https://doi.org/10.1016/S0143-7208(97)00075-2

- Raghavacharya C. (1992) Colour removal of acid dye from individual effluent - a comparative review of available technologies. Chem. Eng. World Vol.32: 53 – 54

- Pak D and Chang W (1999) Decolourising dye wastewater with low temp. Oxidation Water Science Tech. Vol.40:115 – 121

https://doi.org/10.1016/S0273-1223(99)00492-8

- Claire M., (1998) JSDC Vol.114 :118

- Banat I.M and Mcmullan G. (1999) Microbial decolourisation of textile dyes present in textile industries effluent. In proceeding of the industrial waste technical conference U.S.A, 1 – 6

- Ogutveren U.B and Kaparal S (1994) Colour removal from textile effluent by electrochemical destruction. Journal of Environ. Sci. Health. Vol.29:1 – 16

- Misihra G and Tripathy M (1993) Annual review of the treatments for decolourisation of textile effluent. Colourage Vol.40: 53 – 58

https://doi.org/10.1016/j.chemosphere.2018.06.043

- Choy K.R.H and Mckay G. (1999) Sorption of acid dyes from effluents using activated carbon. Resource Conserv. Recy. Vol.27: 17 – 71

https://doi.org/10.1016/S0921-3449(98)00085-8

- Kumar M.N.V.R, Sridhari T.R and Bharani K.D (1998) Trends in colour removal from textile mill effluents. Colourage Vol.40: 25 – 34

- Nasser N.M and El-Geundi M. (1991) Comparative cost of colour removal from textile effluent using natural adsorbent. J. Chem. Tech. Bio. Tech Vol.50:257 – 264

doi:10.1002/jctb.280500210

- Poots V.J.P., Mckay J.J (1976A) The removal of acid-dye from effluent using natural adsorbent Peat. Water Res. Vol.10:1031 – 1066

https://doi.org/10.1016/0043-1354(76)90037-3

- Poots V.J.P., Mckay J.J (1976A) The removal of acid-dye from effluent using natural adsorbent wood. water Res. Vol.10:1067 – 1070

https://doi.org/10.1016/0043-1354(76)90037-3

- Gupta G.S., Prasad G and Singh V.H (1990) Removal of chrome dye from aqueous solutions by mixed adsorbents: fly-ash and coal. Water Resources. Vol.10:24 - 50

doi: 10.1016/0043-1354(90)90063-c

- Prof. F.E Okieimen. A book on physical chemistry, Basic University series

- Wiley J. (1983) Encyclopedia of Chemical Technology. Wileys interscience publication. Vol.1(3): 531 – 536

- Perry R.H and Green D. Chemical Engineers Handbook 6th edition. Macgraw Hill International Book Company. : 5 – 16

- Anozie A.N., Ezomo F.A.S. and Emofurieta W.O. Bleaching performance of some Nigeria clays, Journal of mining and geology. Vol.29(1) 57 – 62

- Anderson A.J.C (1962) Refining of oils and fats. Pergamon press, London : 92 – 103

- Faust D.S and Aly M.O (2018) Chemistry of wastewater treatment, Butterworths, Boston

https://doi.org/10.1201/9781315139265.

- Malik P.K (2004) Dye removal from wastewater using activated carbon developed from sawdust: Adsorption equilibrium and kinetics. Journal of hazardous materials B113 (1 - 3): 81 – 88

doi: 10.1016/j.jhazmat.2004.05.022

- Dawid M. and Stanislaw C (2014) Statistical analysis of adsorption experimental data – influence of the selection of error function on optimized isotherm parameters. Annales Universitatis mariae curie-sklodoroska section AA-chemia 68(1 - 2)

doi: 10.2478/umcschem – 2013 – 0006.

- Wang S., Zhu Z.H., Coomes A., Haghseresht F and Lu G.O (2005) The physical and surface chemical characteristics of activated carbon and the adsorption of methylene blue from wastewater. Journal of Colloid interface science Vol. 284: 440 - 446