Review Article

Agro-Derived Nanomaterials via Green Synthesis for Preventive Health and Disease Control: Mechanistic Insights and Challenges

Abstract

The rising global burden of infectious diseases, antimicrobial resistance (AMR), and the need for safer alternatives to synthetic health protective materials have driven intense research into bioactive nanomaterials. Agriculturally based nanomaterials (ABNMs), such as AgNPs, CuNPs, ZnO, nanocellulose, and biochar, are enriched with phytochemical residues or organic functional groups, further enhancing their biological potency. This study aims to provide a comprehensive understanding of how agricultural resources can be strategically leveraged to produce nanomaterials that are viable for various health security strategies. The general mechanism of ABNMs preparation includes chelation of metal ions by phytochemicals, redox-driven nucleation of metal atoms, growth and coalescence of nanocrystals, and surface passivation by biomolecular residues. These findings identify the recent multifunctional applications of ABNMs in one health approaches. They have been applied in disease prevention and the protection of plant crops, the environment, animals, and humans, through mechanisms such as antimicrobial activity, immunomodulation, targeted delivery of bioactive compounds, hormetic physiological stimulation, and environmental detoxification. However, critical challenges remain. Reports on in vivo safety, long-term ecotoxicological impacts, and interactions with soil microbiota are limited. Therefore, we underscore the necessity of comprehensive life-cycle assessments, environmental fate studies, and dose-response toxicological evaluations to balance the technological advantages of agro-derived nanomaterials with environmental and health safety considerations. Addressing the identified limitations, especially those related to reproducibility, scalability, and comprehensive toxicity evaluation, will be fundamental to unlocking their full potential in one health approaches.

Keywords: Nanomaterials; Green Synthesis; Biomolecules; Mechanisms; One Health; Prophylaxis; Antimicrobial; Immunomodulatory

1. Introduction

Agricultural systems generate a diverse range of biological materials, including leaves, bark, fruit peels, seeds, husks, stems, root extracts, plant exudates, and agro-processing residues, which are rich in secondary metabolites, polysaccharides, proteins, alkaloids, and phenolic compounds. Over the past decade, these biomolecules have become essential precursors for the synthesis of agriculturally based nanomaterials (ABNMs) via green or biogenic processes. Unlike conventional chemical or physical nanoparticle fabrication methods, agricultural resources offer intrinsic reducing and stabilizing agents, operate under mild reaction conditions, align with the principles of the circular economy, and promote sustainable development (John et al., 2025; Priya et al., 2023). As a result, ABNMs have emerged as a promising class of nanomaterials with significant applications in disease prevention, spanning biomedical, pharmaceutical, food packaging, agricultural protection, and environmental health contexts (Adetunji et al., 2021; Ahmed et al., 2021; Kheiriabad et al., 2024; Pathakoti et al., 2019).

The rising global burden of infectious diseases, antimicrobial resistance (AMR), and the need for safer alternatives to synthetic antimicrobials have driven intense research into bioactive nanomaterials (Iqbal et al., 2026; Mmbando et al., 2025; Rahman et al., 2024). Nanoparticles synthesized from agricultural feedstocks, such as plant-mediated silver nanoparticles, zinc oxide nanoparticles derived from crop residues, nanocellulose from agricultural fibers, or carbon-based nanomaterials derived from husks and fruit peels, have demonstrated broad-spectrum antibacterial, antiviral, antifungal, antiparasitic, and immunomodulatory activities (Murugan et al., 2025). These properties stem from physicochemical characteristics, such as high surface-area-to-volume ratios, unique surface chemistries, the generation of reactive oxygen species (ROS), ion release, and surface interactions with microbial membranes (Agarwalla et al., 2023; Díez-Pascual, 2020; Harish et al., 2022). Notably, many ABNMs are enriched with phytochemical residues or organic functional groups, which further enhance their biological potency. Research over the last several years has indicated that ABNMs can inhibit Staphylococcus aureus, Escherichia coli, Pseudomonas aeruginosa, fungal pathogens such as Candida spp., and phytopathogens including Fusarium, Alternaria, and Xanthomonas (Gandhi et al., 2018; Rotimi et al., 2019; Ruangtong et al., 2020). In the biomedical sector, they are being explored for wound healing, disease prophylaxis, vaccine adjuvant development, food preservation, and antimicrobial coatings (Adetunji et al., 2021; Banerjee et al., 2021). In agriculture, ABNMs are utilized for seed protection, nano-enabled pesticide delivery, suppression of soil pathogens, and enhancement of crop disease resistance (Javaid et al., 2024). Their versatility derives from the ability to tune particle size, morphology, crystallinity, surface charge, and composition by simply altering the agricultural biomass source or synthesis conditions (Barhoum et al., 2020).

However, regulatory frameworks for biogenic nanoparticles are still emerging, and most applications remain at the laboratory scale, with few translational or commercialized examples. Nevertheless, the field is advancing rapidly due to the convergence of sustainable nanotechnology, biomaterial valorization, plant chemistry, and infectious-disease research. Studies emphasize the promise of biogenic and ABNMs for biomedical and agricultural applications, underscoring their antimicrobial potency, lower toxicity compared to chemically synthesized analogues, and environmental benefits (Adetunji et al., 2021; Törős et al., 2025). Other recent studies highlight their ability to modulate immune responses, act as antiviral agents, and provide new avenues for tackling antimicrobial resistance. Given the urgent need for sustainable and potent disease-prevention technologies, a focused and integrative review is timely. This article synthesizes current knowledge on agriculturally derived nanomaterials, emphasizing green synthesis routes, mechanistic pathways underlying antimicrobial and antiviral activity, biomedical and agricultural applications, safety and environmental considerations, and translational and regulatory challenges. By consolidating these domains, we aim to provide a comprehensive understanding of how agricultural resources can be strategically leveraged to produce nanomaterials for applications in One Health strategies.

2. Diseases, Causes, and Transmission Pathways

The efficacy of agriculturally based nanomaterials in disease prevention is significantly influenced by the nature of the diseases, their impacts, and the approaches used to address them sustainably (Fu et al., 2020). Diseases are broadly defined as any condition that impairs normal functioning and are primarily classified as infectious or non-infectious (Mba & Nweze, 2022). Communicable diseases are caused by pathogenic microorganisms, including bacteria, viruses, fungi, and parasites, and can be transmitted directly or indirectly from one organism to another (Meena et al., 2019; Paul, 2024). Non-infectious diseases, on the other hand, arise from genetic, physiological, environmental, or lifestyle factors and are not contagious.

The impact of diseases on health systems, agriculture, and economies is profound and multifaceted (Rich & Perry, 2011; Smith et al., 2019). Infectious diseases can overwhelm health systems, as seen during the COVID-19 pandemic, requiring significant resources for treatment, quarantine, and vaccination (Akande & Akande, 2020; Filip et al., 2022). Non-infectious diseases, such as cardiovascular diseases and cancers, also place a substantial burden on healthcare infrastructure (Farringtonargue, 2012). In agriculture, both infectious and non-infectious diseases lead to significant crop and livestock losses, threatening food security and livelihoods (Yasmin et al., 2024). Economically, diseases can trigger market instability, reduce productivity, and increase healthcare costs (Benatar et al., 2013). For instance, outbreaks of zoonotic diseases can disrupt international trade and tourism, leading to severe economic repercussions (Banik & Basu, 2025).

Microbial contamination in food and water systems is a significant cause of disease outbreaks worldwide (Rath, 2021). Contamination can occur at various stages, from agricultural production to processing, distribution, and storage (Kumar et al., 2020). Inadequate sanitation and hygiene practices, particularly in developing countries, contribute to the spread of waterborne diseases such as cholera, typhoid fever, and dysentery (Ashbolt, 2004). Foodborne illnesses, including salmonellosis, E. coli infections, and listeriosis, are often linked to contaminated produce, meat, and dairy products (Gourama, 2020). Suboptimal storage conditions, particularly poor regulation of temperature and relative humidity, create favorable environments for spoilage microorganisms and mycotoxin-producing fungi to proliferate, thereby increasing food safety risks (Mannaa & Kim, 2017). In agricultural systems, the inappropriate application of pesticides and fertilizers can disrupt beneficial soil microbial communities, weakening natural disease-suppression mechanisms and increasing crop vulnerability to pathogenic infections (Baweja et al., 2020). Additionally, the growing prevalence of antimicrobial resistance (AMR) in agricultural settings has been strongly associated with excessive antibiotic use in livestock production. This practice facilitates the transmission of resistant bacteria to humans through food products, environmental dissemination, and direct contact (Endale et al., 2023; Hazards et al., 2021).

Cross-species transmission remains a central concern in disease ecology, as zoonotic pathogens, capable of spreading from animals to humans, account for a substantial proportion of newly emerging infectious diseases globally (Mackenzie et al., 2007). Intensified livestock production systems and increased human–animal interactions significantly elevate the likelihood of zoonotic spillover events. These risks are further amplified by wildlife trade, habitat encroachment, and ecosystem disruption, which expose human populations to previously unencountered pathogens (Magouras et al., 2020). Environmental contamination also plays a critical role in accelerating the development of AMR and disease transmission. Pollutants such as heavy metals, agricultural runoff, and industrial effluents contaminate aquatic ecosystems, creating selective pressures that favor the emergence and persistence of antimicrobial-resistant microorganisms (Endale et al., 2023).

Addressing the shortcomings of conventional disease prevention strategies requires an integrated, multi-disciplinary approach that combines technological innovation, sustainable agricultural practices, and supportive policy frameworks (Rawal & Acharya, 2024). Notably, conventional interventions such as broad-spectrum antibiotics and synthetic agrochemicals often result in unintended environmental degradation and the development of microbial resistance (Oladunjoye et al., 2022). In contrast, emerging technologies, particularly nanotechnology, offer precision-based disease prevention and control strategies with reduced off-target effects. The strategic integration of nanotechnology into sustainable agricultural and health systems represents a promising avenue for mitigating disease risks, enhancing biosecurity, and promoting long-term environmental, economic, and public health resilience.

3. Green and Biogenic Synthesis of Nanomaterials from Agricultural Feedstocks

Green synthesis of nanomaterials using agricultural substrates hinges on the capacity of biomolecules to convert metal ions or precursor compounds into stable nanoparticles under environmentally benign conditions (El-Hussein et al., 2024). In contrast to conventional chemical reduction, which often requires toxic reagents such as hydrazine and sodium borohydride, high-energy inputs, and controlled atmospheres, agriculturally mediated synthesis is typically performed in aqueous media at low temperatures and ambient pressure (Nasrollahzadeh et al., 2019; Zamani et al., 2019). Extracts obtained from leaves, fruit peels, seeds, or agro-processing residues serve as reducing agents to initiate the conversion of metal ions to zero-valent or oxide forms and capping agents to stabilize emerging nanocrystals and prevent aggregation (Javed et al., 2020).

As shown in Figure 1, the general mechanism includes chelation of metal ions by phytochemicals, redox-driven nucleation of metal atoms, growth and coalescence of nanocrystals, and surface passivation by biomolecular residues (Tiwari et al., 2024). Biomolecules such as phenolics, tannins, and reducing sugars are particularly active in redox processes, while proteins and polysaccharides confer steric and electrostatic stabilization (Xiao et al., 2023). Reaction parameters, including pH, precursor concentration, extract composition, incubation time, and temperature, strongly influence the nucleation–growth balance, particle morphology, and overall biological activity of the resulting nanomaterials (Hachem et al., 2022; Thanh et al., 2014). The use of abundant agri-waste for the synthesis of nanomaterials promotes cost-effectiveness, tailored particle features, diversity, sustainability, and bio-functionality of nanomaterials (Ranganathan et al., 2020; Verma et al., 2025). Chelation stabilizes the metal ions in solution. It positions phytochemicals close enough to donate electrons during the reduction step, as well as controlling reaction kinetics and influences nanoparticle size (Gebre, 2023; Kaur et al., 2024) Chelation happens when the functional groups (–OH, –COOH, –NH₂, –C=O) in phytochemicals such as, polyphenols (flavonoids, tannins), organic acids (citric, malic acids), alkaloids, proteins, amino acids and sugars, from agricultural extracts (leaves, peels, seeds, roots, etc.) bind (chelate) with positively charged metal ions (e.g., Zn²⁺, Fe³⁺, Ni²⁺, Ag⁺, Au³⁺) (Jacob et al., 2024; Nobahar et al., 2021). For example, flavonoids donate electrons from their hydroxyl groups and bind to Fe³⁺ to form a metal–ligand complex in stepwise reactions involving deprotonation of the hydroxyl group and coordination with Fe3+. Redox-driven nucleation of metal atoms determines particle size distribution. Fast nucleation leads to small nanoparticles, while slow nucleation yields larger, polydisperse particles (Zhang et al., 2012). After chelation, phytochemicals, such as polyphenols (catechins, gallic acid), vitamin C (ascorbic acid), and sugars (glucose, fructose), act as reducing agents, converting metal ions (Mn⁺) into neutral atoms (M⁰) via electron donation (Abbasi et al., 2014; Ovais et al., 2018). Once enough M⁰ atoms form, they cluster together to form nuclei.

Figure 1: Mechanism of Green Synthesis of Nanomaterials

Growth and coalescence of nanocrystals determine the shape (spherical, cubic, rod-like) and crystallinity of the final nanomaterial. These could be influenced by factors like phytochemical concentration, temperature, pH, and metal ion concentration (Cozzoli & Manna, 2007). After the initial formation of nuclei, more metal atoms deposit on these nuclei, leading to crystal growth (incremental deposition) and coalescence (small nanoparticles merging into larger crystallites) (Wen, 2020). However, plant biomolecules regulate growth rate, particle morphology, and crystal plane orientation (De Yoreo, 2010). Surface passivation prevents agglomeration (nanoparticles stay separate), provides colloidal stability, may introduce functional groups for catalytic or sensing activity, influences nanoparticle charge (zeta potential), enhances biocompatibility, and reduces toxicity (Guerrini et al., 2018). Phytochemicals not only reduce metal ions, but they also adsorb onto nanoparticle surfaces through biomolecular compounds, like proteins, polysaccharides, phenolic compounds, and amino acids. These molecules stay attached as a capping or stabilizing layer (Elshafie et al., 2023). Therefore, strongly influencing reactivity, dispersibility in water, photocatalytic and antimicrobial performance, as well as magnetic properties in the case of ferrites.

4. Phytochemicals and Biomolecules from Agricultural Materials

Agricultural biomass, comprising plant extracts, fruit and vegetable peels, leaves, bark, seeds, roots, stems, husks, shells, crop residues, and agro-industrial waste, provides a chemically rich platform for synthesizing nanomaterials through green, biogenic, and sustainable approaches (Bhargava et al., 2024; Nguyen, 2017). These biologically mediated processes rely on the intrinsic reducing, stabilizing, and capping capabilities of phytochemicals and biomolecules naturally present in agricultural materials, including flavonoids, tannins, alkaloids, terpenoids, amino acids, sugars, organic acids, and enzymes (Acharya et al., 2025; Elshafie et al., 2023) (Figure 2).

Figure 2: Phytochemicals and Biomolecules from Agricultural Materials

5. Synthesis Routes of Agriculturally Derived Nanomaterial

5.1 Use of Plant Extracts, Phytochemicals, Agro-Industrial Waste, and Crop Residues

Plant organs, such as leaves, bark, and flowers (Figure 3), are a rich source of phenolic compounds, flavonoids, terpenoids, and alkaloids, which play critical roles in nanoparticle formation. Leaf extracts, such as those from Moringa, Azadirachta indica (neem), Ocimum sanctum, and Camellia sinensis have been extensively employed to synthesize silver (Ag), gold (Au), copper (Cu), iron oxide (Fe₃O₄), zinc oxide (ZnO), and titanium dioxide (TiO₂) nanoparticles (Anupong et al., 2023; Gandhi et al., 2018; Gupta et al., 2025; Ibrahim, 2015; Rigopoulos et al., 2019; Rotimi et al., 2019; Ruangtong et al., 2020; Saod et al., 2022). Bark and flower extracts similarly yield metal nanoparticles, often producing unique morphologies due to their distinctive phytochemical profiles (Kuppusamy et al., 2016). Citrus peels (orange, lemon, grapefruit), banana peels, pomegranate husks, and mango peels are rich in citric acid, pectin, polyphenols, and vitamins that facilitate rapid reduction of metal precursors (Suhag et al., 2023). These wastes also exhibit strong stabilizing properties, yielding well-dispersed nanoparticles with enhanced antimicrobial activity (Kumar et al., 2020). Seeds from papaya, grape, and jackfruit have also been used in nanoparticle synthesis (Patra et al., 2024). Starches and sugars in root crops like cassava, potato, and sweet potato can act as mild reducing agents and steric stabilizers. Their high polysaccharide content produces nanoparticles with smooth surfaces and uniform size distributions (Chang et al., 2017; Plucinski et al., 2021).

Figure 3: Nanoparticles from Plant Extracts, Phytochemicals, Agro-Industrial Waste, and Crop Residues

Agro-industrial waste streams are abundant and inexpensive sources of biomolecules suitable for the generation of nanomaterials (Nath et al., 2023). These include waste from fruit processing industries, vegetable markets, sugar mills, timber operations, and grain agriculture. Several recent works highlight the potential of agro-waste to yield high-value nanomaterials for environmental and biomedical applications (Anupong et al., 2023; Gandhi et al., 2018; Gupta et al., 2025; Ibrahim, 2015; Rigopoulos et al., 2019; Rotimi et al., 2019; Ruangtong et al., 2020; Saod et al., 2022). Rice husk, coconut husk, wheat bran, and corncob fibres contain high silica or carbon content, enabling the synthesis of silica nanoparticles, carbon dots, or activated carbon nanomaterials (Chakroborty et al., 2023). Also, coconut, groundnut, and walnut shell wastes are pyrolyzed to form biochar, which is then converted into carbon-based nanomaterials or nanocomposites with unique adsorptive and antimicrobial properties (Aslam et al., 2025; Devi et al., 2024). Fruit processing wastes, such as pulp residues and discarded fruit matter from juice industries (mango, papaya, apple, citrus), contain abundant polyphenols and organic acids. These compounds are particularly effective in stabilizing metal nanoparticles during aqueous or hydrothermal synthesis. Sugarcane bagasse is a lignocellulosic biomass widely used to produce nanocellulose, carbon nanostructures, and metal oxide nanocomposites (Mohammed et al., 2024). Molasses, rich in sugars and organic acids, has also been used as a reducing medium for synthesizing metal nanoparticles (Manjari et al., 2020).

5.2 Biogenic Synthesis Using Microbial Systems Associated with Agriculture

Agricultural environments host diverse microbial communities, bacteria, fungi, and yeasts that possess enzymatic machinery capable of nanoparticle biosynthesis (Figure 4). These biological systems reduce metal ions intracellularly or extracellularly, producing nanoparticles that are often highly uniform and exhibit distinctive surface coatings composed of biomacromolecules. Soil bacteria, such as Bacillus, Pseudomonas, and Rhizobium spp., can produce metal nanoparticles via enzymatic reduction (Ali et al., 2019; Iravani & Varma, 2020). The cell walls and secreted proteins stabilize the nanoparticles, preventing aggregation. Filamentous fungi (e.g., Aspergillus, Trichoderma, Penicillium) are widely used due to their high metal tolerance and large biomass (Narayanan & Sakthivel, 2010).

Figure 4: Biological Materials in Nanoparticle Preparation

Their extracellular metabolites support rapid metal ion reduction and nanoparticle stabilization, yielding monodisperse metal and metal oxide nanoparticles (Iravani & Varma, 2020). Yeasts and microalgae from agricultural wastewaters and irrigation channels also facilitate nanoparticle biosynthesis via enzymatic pathways, sometimes incorporating biomineralization mechanisms (Hulkoti & Taranath, 2014).

5.3 Carbon-Based Nanomaterials from Biomass

Carbon nanomaterials, such as carbon dots (CDs), graphene-like sheets, carbon nanotube-like structures, and biochar-derived nanoparticles, are increasingly synthesized from agricultural waste (Al Hunaiti et al., 2025; Zulfiqar et al., 2024). Biomass rich in lignin, cellulose, and hemicellulose (rice husk, coconut shell, sugarcane bagasse) undergoes pyrolysis, hydrothermal carbonization, or laser ablation to produce these materials (Ashour et al., 2025; Chand et al., 2025; Tohamy et al., 2025). Carbon dots derived from fruit peels or vegetable waste often retain surface functional groups (–OH, –COOH), which enhance their water solubility and make them suitable for antimicrobial, antioxidant, and biosensing applications.

5.4 Nanocellulose Extraction from Agricultural Fibers

Agricultural fibers such as sugarcane bagasse, cotton linters, wheat straw, jute, and banana fibers are excellent sources of nanocellulose, specifically cellulose nanocrystals (CNCs) and cellulose nanofibers (CNFs). Acid hydrolysis, mechanical fibrillation, enzymatic digestion, or TEMPO-mediated oxidation is used to isolate nanoscale cellulose structures with high crystallinity and tensile strength (Gamelas et al., 2015; Isogai et al., 2011; Li et al., 2015; Rohaizu & Wanrosli, 2017). Nanocellulose has been incorporated into hydrogels, films, antimicrobial composites, packaging materials, and wound dressings. Its biodegradability, non-toxicity, and adaptability make it a valuable platform for disease-prevention technologies (Shaji et al., 2025; Vasile et al., 2025).

5.5 Metal and Metal Oxide Nanoparticles from Agricultural Extracts

Among all synthesized nanomaterials from agricultural extracts (Figure 4), silver nanoparticles are the most extensively studied due to their potent and broad-spectrum antimicrobial properties. Plant-mediated AgNPs often exhibit enhanced biological activity because of phytochemical surface residues (Anupong et al. 2023, Gupta et al. 2025). Although less potent as antimicrobials compared to AgNPs, AuNPs synthesized using plant extracts are valued for their stability, biocompatibility, and tunable shapes (spheres, rods, stars), which enable them to excel in sensing, imaging, and drug delivery applications (Rotimi et al. 2019). ZnO nanoparticles are widely synthesized using agricultural extracts from leaves, peels, and roots (Ruangtong et al. 2020). Their antimicrobial performance is attributed to ROS generation, zinc ion release, and membrane interactions. ZnO NPs also exhibit UV-blocking properties, making them suitable for active packaging and protective films.

Cu-based nanoparticles synthesized from agro-waste extracts deliver vigorous antimicrobial activity at a lower cost compared to silver. Their applications range from antifungal agents to agricultural nanofungicides (Aswini et al., 2024). Iron oxide nanoparticles derived from plant extracts are widely used in magnetic separation, antimicrobial formulations, biosensing, and targeted drug delivery (Tyagi et al., 2021). TiO₂ nanoparticles synthesized from agricultural extracts emphasize photocatalytic antimicrobial activity, especially under UV or visible light (Gandhi et al., 2018).

5.6 Hybrid and Nanocomposite Materials

Agricultural feedstocks enable the synthesis of multifunctional nanocomposites by combining metal nanoparticles with biopolymers such as starch, chitosan, pectin, and cellulose. Examples include: AgNP-containing nanocellulose films for wound care and food packaging; ZnO-containing pectin nanocomposites; carbon–metal nanocomposites for antimicrobial coatings; biopolymer-stabilized nanopesticide formulations for crop protection (Al Hunaiti et al., 2025; Aswini et al., 2024; Zulfiqar et al., 2024). Nanocomposites often exhibit synergistic effects, enhancing stability, mechanical properties, and antimicrobial activity.

6. Basic Methods in Synthesising ABNMs

Various interesting methods have been employed to synthesize nanomaterials with biological relevance. These methods are usually selected based on the expected product quality and the advantages of each technique. Figure 5 depicts the various methods.

Figure 5: Basic Methods Employed for Synthesising Agro-Nanomaterials

6.1 Acid Hydrolysis

Acid hydrolysis is a chemical method used to selectively cleave the amorphous regions of lignocellulosic biomass, leaving behind highly crystalline nanostructures such as cellulose nanocrystals (CNCs) (Habibi et al., 2010). Strong mineral acids (commonly sulfuric or hydrochloric acid) penetrate the cellulose fibers, hydrolyzing glycosidic bonds in less-ordered domains while preserving crystalline segments (Klemm et al., 2011). Although this method produces nanomaterials with high crystallinity and uniform dimensions, it often introduces surface sulfate or chloride groups and generates acidic waste streams that require careful neutralization and disposal (Gamelas et al., 2015).

6.2 Enzymatic Digestion

Enzymatic digestion employs cellulolytic enzymes (e.g., endoglucanases and cellobiohydrolases) to degrade cellulose fibers under mild, environmentally benign conditions (Pääkkö et al., 2007). The enzymes preferentially act on amorphous regions of cellulose, facilitating fibril separation while minimizing structural damage to crystalline domains (Brinchi et al., 2013). This method is considered highly sustainable but is limited by enzyme cost, longer processing times, and sensitivity to reaction conditions such as pH and temperature (Li et al., 2015).

6.3 Hydrothermal Carbonization

Hydrothermal carbonization (HTC) is a wet-chemical conversion technique conducted at moderate temperatures (180–250 °C) and autogenous pressures, making it particularly suitable for moisture-rich agricultural residues (Titirici & Antonietti, 2010). During HTC, biomass undergoes dehydration, decarboxylation, and polymerization reactions, yielding hydrochar nanoparticles with oxygen-containing functional groups (Sevilla & Fuertes, 2009). This method allows precise control over particle morphology and surface chemistry without the need for prior drying of feedstocks (Tohamy et al., 2025). ABNMs produced via HTC are increasingly explored for energy storage, pollutant adsorption, and controlled nutrient delivery in sustainable agriculture.

6.4 Ionic Gelation

Ionic gelation is a mild, solvent-free technique commonly employed for the synthesis of biopolymer-based nanomaterials, particularly those derived from agro-resources such as chitosan, alginate, pectin, and carrageenan (Rinaudo, 2006). The process involves electrostatic interactions between oppositely charged biopolymers and multivalent counter-ions (e.g., Ca²⁺, Zn²⁺, or tripolyphosphate), leading to spontaneous nanoparticle formation under ambient conditions (Calvo et al., 1997). In ABNMs applications, ionic gelation enables the encapsulation of bioactive compounds, nutrients, or antimicrobial agents, facilitating controlled release and enhanced stability (Rinaudo, 2006). The simplicity, low energy requirement, and avoidance of toxic reagents make ionic gelation highly attractive for sustainable agricultural, food, and biomedical nanotechnology.

6.5 Laser Ablation

Laser ablation is a physical, top-down synthesis approach in which high-energy laser pulses irradiate a solid agro-derived precursor or a target immersed in a liquid medium, leading to the formation of nanoparticles through rapid vaporization and condensation (Zhang et al., 2017). When applied to ABNMs synthesis, laser ablation offers the advantage of producing ultra-pure nanomaterials without the use of chemical reducing agents or stabilizers (Amendola & Meneghetti, 2009). The size and crystallinity of the nanoparticles can be tuned by adjusting laser wavelength, pulse duration, and surrounding medium (Chand et al., 2025). Although scalability remains a challenge, this technique is valuable for producing well-defined nanomaterials for biomedical and environmental applications.

6.6 Mechanical Fibrillation

Mechanical fibrillation relies on intense physical forces, such as high-pressure homogenization, grinding, or ultrasonication, to delaminate cellulose fibers into nanoscale fibrils (Siró & Plackett, 2010). This approach preserves the native chemical structure of cellulose while producing cellulose nanofibrils (CNFs) with high aspect ratios and entangled morphologies (Nechyporchuk et al., 2016). However, the method is energy-intensive and often requires pretreatment steps to reduce energy consumption and improve fibrillation efficiency (Isogai et al., 2011).

6.7 Pyrolysis

Pyrolysis is a thermochemical conversion process in which agricultural biomass is decomposed at elevated temperatures (typically 300–800 °C) under an oxygen-limited or inert atmosphere (Joseph, 2015). In ABNMs synthesis, pyrolysis is primarily used to generate biochar and carbon-based nanomaterials with high surface area, tunable porosity, and abundant surface functional groups (Verma et al., 2023). Feedstock composition (e.g., lignin, cellulose, and hemicellulose content) and operational parameters, such as heating rate and residence time, strongly influence the physicochemical properties of the resulting nanomaterials (Ashour et al., 2025). Pyrolysis-derived ABNMs have found extensive use in environmental remediation, catalysis, and soil amendment due to their stability and adsorption capacity.

6.8 TEMPO-mediated Oxidation

TEMPO-mediated oxidation is a selective chemical modification technique that converts primary hydroxyl groups on cellulose into carboxylate groups using a TEMPO/NaBr/NaClO catalytic system (Isogai et al., 2011). This surface functionalization introduces electrostatic repulsion between fibrils, enabling efficient individualization of cellulose nanofibrils with reduced mechanical energy input (Isogai, 2020). The resulting nanomaterials exhibit enhanced dispersibility, reactivity, and suitability for biomedical and environmental applications, though careful control of reaction conditions is required to avoid excessive depolymerization (Rohaizu & Wanrosli, 2017).

7.0 Some Recent ABNMs for Disease Prevention

The studies represented in Table 1 collectively demonstrate the growing versatility of agriculturally derived materials as sustainable precursors for nanoparticle synthesis, with applications spanning antimicrobial therapy, antimalarial interventions, photocatalytic degradation of pollutants, and environmental remediation. Silver nanoparticles (AgNPs) remain the most frequently synthesized nanomaterials, mainly due to their broad-spectrum antimicrobial efficacy against Gram-positive and Gram-negative bacteria, fungi, and parasites. Extracts from Euphorbia cotinifolia, Artemisia spp., banana peels, citrus peels, green tea, and Curcuma longa consistently produced AgNPs capable of inhibiting pathogens such as Escherichia coli, Staphylococcus aureus, Klebsiella pneumoniae, and Plasmodium falciparum (Anupong et al., 2023; Gandhi et al., 2018; Gupta et al., 2025; Ibrahim, 2015; Rigopoulos et al., 2019; Rotimi et al., 2019; Ruangtong et al., 2020; Saod et al., 2022). The repeated selection of AgNPs reflects both their well-established biocidal mechanisms, such as membrane disruption, reactive oxygen species (ROS) generation, and enzyme inhibition, and the ease with which plant phytochemicals can reduce Ag⁺ ions under mild conditions.

Table 1: Some Agro Materials Employed in Synthesizing NPs, and Their Applications

| Agricultural Materials | Nanoparticle | Synthesis Method | Target pathogens | Application | References |
| --- | --- | --- | --- | --- | --- |
| Banana peel extract | AgNPs | 50 ml of Aqueous AgNO3 (1 mM) + 1 ml of BPE (equivalent to 6.8 mg dry weight) and incubated in the dark at 30 °C under static conditions. | - | Antimicrobial activity | Ibrahim (2015) |
| Momordica charantia leaf aqueous extract | TiO2NPs | - | Anopheles Stephensi Liston, Plasmodium falciparum | Antimalarial activity | Gandhi et al. (2018) |
| Callistemon citrinus (C. citrinus) seed extract | AuNPs | 12.5 mL of extract was added to 90 mL of Gold (III) Chloride solution (0.001M), followed by incubation for 6h with continuous stirring in the dark. | Plasmodial parasite | Antimalarial activity | Rotimi et al. (2019) |
| Banana peel extract | AgNPs | Silver nitrate (AgNO3) and BPE concentrations (0.25-2.25 mM, 0.2-1.96 % v/v, respectively), incubation period (24-120 h) | Escherichia coli and Staphylococcus aureus | Antibacterial and antioxidant activities | Rigopoulos et al. (2019) |
| Artemisia species (A. abrotanum and A. arborescens) | AgNPs | 100 mL of the hydroalcoholic extracts were diluted to 500 mL with milliQ water and slowly added to a 500 mL water solution of AgNO3 (340 mg) to reach a final molarity of 2 mM, under magnetic stirring at room temperature. | Plasmodium falciparum | Antimalarial activity | Avitabile et al. (2020) |
| Banana peel crude extract | ZnONPs | 100 mL of plant extract was added to 50 mL of zinc acetate solution (0.2 M) and stirred for 1 h using a magnetic stirrer. | Bacillus subtilis, Staphylococcus epidermidis, Escherichia coli Skin cancer cell, colorectal cancer cell, and liver cancer cell | Antibacterial and anticancer activities | Ruangtong et al. (2020) |
| Spinacia oleracea (spinach) leaf and Musa acuminata (banana) peel extract | FeNPs | SLE-FeNPs: 0.1 M FeCl3 solution mixed with aqueous SLE in a 2:1 volume ratio at 60°C for 30 minutes with continuous magnetic stirring till the appearance of black colour. BPE-FeNPs: 0.1 M FeCl3 solution mixed with aqueous BPE (supernatant at ambient temperature), hand-shaken for 1 minute, and allowed to sit at room temperature for 1 hour. | Bacillus subtilis, Escherichia coli | Antibacterial activity | Tyagi et al. (2021) |
| Monsonia burkeana plant extract | ZnFe2O4NPs | Hydrothermal | Methylene blue and sulfisoxazole | Photocatalytic activity | Makofane et al. (2021) |
| Orange peel waste | SeNPs | Peel extract (10 mL) was added to 90 mL of 2 mM Na2SeO3, mixed thoroughly, and incubated on a rotary shaker in the dark for 3 h to obtain a homogeneous mixture. The generated Se-NPs were then separated and purified using D.W. and centrifugation. | S. aureus, Pseudomonas aeruginosa, E. coli, K. pneumonia | Antibacterial and antibiofilm | Salem et al. (2022) |
| Green tea | MnONPs | Green tea extract (10 mL, 100 µg/mL in distilled water) was mixed with 100 mL of 0.1 M MnSO4 stock. | Escherichia coli, Klebsiella pneumoniae, Pseudomonas aeruginosa | Antibacterial activity | Saod et al. (2022) |
| Curcuma longa | AgNPs, ZnONPs | 25 ml of 0.2 M ethanolic solution of AgNO3 was added to 75 ml of curcumin ethanolic extract under vigorous stirring and reflux at 60 °C with the addition of 10 g PVP 40000 | Klebsiella pneumonia, Staphylococcus aureus, Pseudomonas aeruginosa, Escherichia coli, Proteus vulgaris, Staphylococcus aureus, Enterococcus faecalis Acinetobacter baumannii | Antibacterial bioassay | El-Kattan et al. (2022) |
| Origanum majorana | ZnO NPs | 10 mL of aqueous leaf extract was added to 90 mL AgNO3 solution (1 mM) and heated to 70°C over a magnetic stirrer for 1 h | E. coli, Klebsiella pneumoniae, Acinetobacter baumannii, Salmonella typhimurium, Enterobacter cloacae, Pseudomonas aeruginosa | Antimicrobial proficiency | Yassin et al. (2022) |
| Green tea | AgNPs | - | Brevibacterium luteolum, Staphylococcus aureus, Pseudomonas aeruginosa, Escherichia coli, | Antimicrobial Bioassay | Hassan Afandy et al. (2023) |
| Ginger and garlic root | TiO2NPs | Various proportions of ginger and garlic were added to 0.1 M (50 mL) titanium ethoxide (Ti4(OCH2CH3)16 ) with stirring, the pH was adjusted to 12 with 2.0 M NaOH, and the mixture was stirred for 2 h at 90 °C until precipitates formed. | Staphylococcus aureus | Antibacterial assessment | Ul-Hamid et al. (2023) |
| Sargassum tenerrimum, a marine seaweed crude extract | AgNPs | 25 mL of extract was mixed with 75 mL of 1 mM AgNO3 solution, stirred continuously with a magnetic stirrer for 4 h in a dark room at 37 °C. The solution changed from dark green to a golden yellow Ag nanoparticles | P. falciparum, P. berghei | Antimalarial activity | Veeragoni et al. (2023) |
| Banana peel and date seed extracts | ZnONPs | 95 mL of zinc acetate dihydrate solution (0.01 M) was mixed with 5 mL of each extract separately. Both mixtures were heated with continuous shaking until a color change and powdery precipitates appeared (70 °C, 1 h), and dried at 60 °C overnight to obtain dry powder | Staphylococus aueus, Bacillus subtilis, Escherichia coli, Salmonella enteritidis | Antimicrobial activity | Hussien (2023) |
| Orange peel aqueous extract | CoNPs | About 90 mL of freshly prepared aqueous extract was blended with 10 mL of freshly prepared 1M Co(NO3)2, heated for 90 min at 60 °C, and kept undisturbed at room temperature overnight. | Escherichia coli, Staphylococcus aureus, Bacillus subtilis, Klebsiella pneumoniae, Aspergillus niger | Antimicrobial and antioxidant activities | Anupong et al. (2023) |
| Leaf extracts of Euphorbia cotinifolia | AgNPs | 1 ml of extract (0.01 mg/ml) is mixed with 90 ml of aqueous AgNO3 (1 mM), diluted to 100 ml with 20 mM Tris–HCl buffer (pH 8), and incubated at room temperature. | P. falciparum | Antimalarial activity | Tiwari et al. (2024) |
| Carica papaya leaf extract | ZnO-CuO Nanocomposite | Sample A: 5 g zinc acetate dissolved in 20 ml of distilled water (DDW), with the addition of 20 ml of leaf extract solution. Sample B: 5 g copper acetate dissolved in 20 ml distilled water (DDW), with the addition of 20 ml leaf extract. A and B are mixed thoroughly using magnetic stirring for 2 h at room temperature, heated in a hot-air oven at 120 °C for 24 h, and centrifuged at 5000 rpm for 15 min. | Staphy lococcus aureus, Klebsiella pneumoniae | Antimicrobial activity | Aswini et al. (2024) |
|  |  |  | Methylene blue dye | Photocatalytic activity |  |
| Azadirachta indica | AgNPs | - | Sclerotinia sclerotiorum and Colletotrichum falcatum, C. gloeosporioides, R. solani | Antifungal analysis | Singh et al. (2024) |
| Citrullus lanatus | ZnONPs | 30 mL of the C. lanatus filtrate was mixed with 30 mL of 1 mM ZnSO4·7H2O, and the mixture was gently shaken until a solution formed. The pH was adjusted to 12 with 1 mM NaOH, and the mixture was centrifuged at 3000 rpm for 5 min. | Pseudomonas spp., Klebsiella spp., Methicillin-resistant Staphylococcus aureus, E. coli, Proteus spp., Yersinia spp., Providencia spp., Morganella spp | Antibacterial Activity | Hayat et al. (2024) |
| Eucalyptus globulus leaves and sugar cane bagasse | Fe3O4/SCB/ biochar | Co-precipitation | Ciprofloxacin | Photocatalytic degradation | Zulfiqar et al. (2024) |
| Organic plant extract (Telia) | TiO2-NiFe2O4-Chitosan Composite | Co-precipitation | Xylene, toluene, 1-methyl naphthalene, and methyl blue dye | Photocatalytic degradation | Al Hunaiti et al. (2025) |
| Citrus sinensis fruit peel extract | AgNPs | 20 ml of citrus peel extract was added to 100 ml of silver nitrate solution (1 mM) in a 250 ml volumetric flask, and the mixture was stirred for 15 min at room temperature using a magnetic stirrer. | staphylococcus aureus, Bacillus subtilis, Escherichiacoli, Salmonella typhi | Antimicrobial and anticancer activity against breast and lung cancer | Gupta et al. (2025) |

In contrast, metal oxide nanoparticles, including ZnO, TiO₂, MnO, Fe₃O₄, Co, and composite ferrites (e.g., ZnFe₂O₄, TiO₂–NiFe₂O₄–chitosan), are more frequently associated with photocatalytic and environmental applications (Gandhi et al., 2018; Ruangtong et al., 2020; Saod et al., 2022; Yassin et al., 2022). These materials demonstrate dual functionality: antimicrobial activity and degradation of organic contaminants, including methylene blue, sulfisoxazole, ciprofloxacin, xylene, and toluene. The inclusion of ferrite-based and composite systems highlights a strategic move toward materials that combine photocatalytic activity with magnetic separability, improving post-treatment recovery and reusability. The consistent success of peel- and waste-derived extracts suggests that waste valorization is a central driver of green nanotechnology, aligning nanoparticle synthesis with circular economy principles. Notably, variations in synthesis parameters, such as extract volume, metal salt concentration, pH, temperature, and incubation time, are shown to influence biological performance. For instance, prolonged incubation or alkaline conditions often enhance nanoparticle crystallinity and antimicrobial efficacy, whereas milder conditions favor smaller particle sizes and improved dispersion.

According to Table 1, several studies focus on antimalarial activity, particularly against Plasmodium falciparum and mosquito vectors such as Anopheles stephensi. Gold nanoparticles (AuNPs) synthesized using Callistemon citrinus seed extract and AgNPs derived from Artemisia species demonstrate the potential of biogenic nanomaterials for the management of parasitic diseases (Avitabile et al., 2020; Gandhi et al., 2018; Hayat et al., 2024; Rotimi et al., 2019; Salem et al., 2022). These findings are particularly relevant in regions with high malaria burden, where plant-derived nanomaterials may offer cost-effective and locally sourced alternatives to conventional therapeutics. In addition, anticancer activity reported for ZnO nanoparticles synthesized from banana peel extract indicates that agriculturally derived nanomaterials may extend beyond antimicrobial roles into preventive and therapeutic biomedical applications, including oncology (Ruangtong et al., 2020). Photocatalytic studies employing ZnFe₂O₄, Fe₃O₄/biochar composites, and TiO₂-based hybrids emphasize the importance of nanocomposite engineering (Al Hunaiti et al., 2025; Aswini et al., 2024; Makofane et al., 2021). The incorporation of biochar, chitosan, or ferrite phases improves charge separation, adsorption capacity, and light utilization. Such multifunctional systems are up-and-coming for simultaneous pathogen inactivation and pollutant degradation, contributing to environmental disease prevention.

8. Mechanisms of Action of Agriculturally Based Nanomaterials in Health Security

Agriculturally derived nanomaterials exhibit unique physicochemical properties, such as high surface area, nanoscale reactivity, biocompatibility, and tunable surface functional groups that enable multiple modes of biological interaction (Agarwalla et al., 2023; Díez-Pascual, 2020; Harish et al., 2022). These attributes underpin their potential as potent disease-preventive agents in plant, animal, and human health (Murugan et al., 2025). The mechanisms by which nanomaterials exert protective effects can be broadly categorized into antimicrobial activity, immunomodulation, targeted delivery of bioactive compounds, hormetic physiological stimulation, and environmental detoxification. According to Howard et al. (2020), these mechanisms vary depending on their composition, synthesis route, surface chemistry, and target organism.

8.1 Targeted Delivery of Bioactive Compounds

Figure 6 shows certain qualities of agriculturally derived nanomaterials, driven by their nanoscale architecture and tunable surface functionalization. These qualities enable them to serve as controlled and targeted delivery systems for antimicrobial agents, nutrients, plant hormones, and therapeutic molecules (Bekah et al., 2025; Karnwal et al., 2024). For example, nanoencapsulated phyto-compounds derived from agricultural waste streams can be targeted to diseased tissues in plants or animals, improving therapeutic efficiency while minimizing environmental impact (Farid, 2025).

8.2 Antimicrobial and Antipathogenic Activity

Agriculturally based nanomaterials synthesized from plant extracts, polysaccharides, proteins, and agricultural waste often contain bioactive phytochemicals that confer strong antimicrobial properties (Li et al., 2023; Sharmin et al., 2021). These nanostructures inhibit pathogenic bacteria, fungi, and viruses through several further mechanisms, as shown in Figure 6. These mechanisms can be explained according to (Miller et al., 2015; Modi et al., 2023).

- Cell membrane disruption: Nanoparticles can adsorb to microbial cell walls, destabilizing membranes, inducing pore formation, and leading to leakage of intracellular contents.

- Generation of reactive oxygen species (ROS): Some nanomaterials catalyze ROS generation, leading to oxidative damage to nucleic acids, proteins, and lipids.

- Enzyme inactivation: Metal and metal-oxide nanoparticles interfere with microbial metabolic enzymes by binding to thiol groups or displacing essential metal ions.

- Inhibition of replication: Nanoparticles may bind to microbial DNA or RNA, preventing replication and transcription.

Many agriculturally derived nanomaterials exhibit synergistic antimicrobial effects that often outperform chemically synthesized counterparts because they contain additional biomolecules, such as polyphenols, flavonoids, and lignin fragments (Lizundia et al., 2021).

8.3 Immunomodulation and Enhancement of Host Defense Systems

Nanomaterials derived from natural agro-resources can modulate innate and adaptive immune responses in plants and animals (Bentrad, 2025). For example, they serve as priming defense pathways in plants, triggering systemic acquired resistance (SAR) and inducing defense-related enzymes such as peroxidases and phenylalanine ammonia lyase (Hönig et al., 2023). In animal systems, they could stimulate cytokine and chemokine production to strengthen immunological surveillance (Liu et al., 2022). In addition, when used in vaccines or prophylactic formulations, biocompatible nanomaterials improve antigen stability, uptake, and immune activation (Vilgelm & Richmond, 2019). These immune-modulating functions make agriculturally based nanomaterials promising for both preventive therapeutics and crop protection.

Figure 6: Mechanisms of Agro-Nanomaterials Actions in Health Security

8.4 Hormetic Effects and Physiological Stimulation

Specific agriculturally based nanomaterials have been reported to enhance physiological processes in low concentrations, triggering hormesis, a beneficial biological response to mild stress (Erofeeva, 2025). They can do so by enhancing antioxidant activity, upregulating stress-response genes, improving photosynthetic efficiency and nutrient uptake in plants, and promoting wound healing and tissue regeneration in animals (Iavicoli et al., 2018). Such physiological enhancements strengthen overall resilience, thereby reducing susceptibility to diseases.

8.5 Environmental Detoxification and Disease Prevention

Agriculturally sourced nanomaterials can also prevent disease indirectly by remediating harmful environmental factors. Their high reactivity and surface chemistry allow them to adsorb or degrade toxins, such as mycotoxins, pesticides, or heavy metals; reduce pathogen prevalence by altering environmental microbial communities; purify water and soil, thereby eliminating disease vectors and contaminants that can compromise plant or animal health (Lin et al., 2024; Rajput et al., 2018; Roy et al., 2022; Zhang et al., 2020). Through environmental detoxification, these nanomaterials contribute to improved ecosystem health, which in turn minimizes disease pressures across agricultural and food systems (Dong et al., 2023). In methods such as adsorption, ABNMs are used as adsorbents to remove pollutants as adsorbates. Another prominent method for environmental remediation is catalysis under light irradiation, which employs nanomaterials as photocatalysts to remove contaminants (Al Hunaiti et al., 2025; Aswini et al., 2024; Zulfiqar et al., 2024).

8.6 Multifactorial and Synergistic Mechanisms

Most agriculturally derived nanomaterials function through multiple pathways, offering synergistic and multi-target disease-prevention effects (Li et al., 2025; Xi et al., 2025). For instance, a plant-extract-synthesized silver nanoparticle may simultaneously display antimicrobial properties, induce immune responses, and enhance antioxidant activity (Chen et al., 2019; Dilshad et al., 2020). This multi-mechanism functionality strengthens their overall potency and makes them ideal candidates for integrated disease management strategies.

8.7 Toxicological Effects of Agro-Derived Nanomaterials

Despite the perception that ABNMs are inherently safer than those produced by conventional chemical methods, toxicological concerns persist for both biological systems and environmental compartments. Even when plant extracts or microbial processes mediate synthesis, metallic and metal-oxide NPs, such as silver (AgNPs) and zinc oxide (ZnO NPs), can induce oxidative stress, cellular damage, and histopathological changes in aquatic and terrestrial organisms at sufficiently high concentrations. For instance, green synthesized AgNPs have been shown to cause significant oxidative damage and altered epidermal functioning in adult zebrafish, compromising integumentary defense mechanisms vital for osmoregulation and survival in aquatic environments. Such effects are consistent with broader findings that nanomaterials can elicit reactive oxygen species (ROS) formation, immune disruption, and cellular impairment in non-target species, including shifts in antioxidant enzyme activities and damage to critical tissues such as gills and liver (Okuthe & Siguba, 2025). Moreover, genotoxicity, such as DNA damage and chromosomal aberrations, remains a documented risk associated with exposure to engineered nanomaterials, even those synthesized through green routes, highlighting that environmentally friendly synthesis does not automatically eliminate biological hazards without careful evaluation of nanoparticle fate and transformation in ecosystems (Okus et al., 2025).

At higher biological scales, toxic responses also extend to mammals, and potentially to humans, when exposure doses exceed safe thresholds. Studies involving rodents have shown that exposure to green-synthesized AgNPs at elevated levels (>50 ppm) can lead to behavioral impairment (e.g., memory dysfunction), altered redox balances in key organs (liver, kidney, spleen, brain), and increased oxidative stress markers, indicating systemic toxicity beyond microbial targets (e.g., hippocampal oxidative damage)(Tarbali et al., 2022). Environmental release of nanoparticles can likewise disrupt ecological communities by affecting beneficial soil and aquatic microorganisms that play pivotal roles in nutrient cycling and ecosystem function. For example, ZnO NPs released into aquatic systems have been associated with impaired algal photosynthesis and detrimental effects on soil microbiota due to ion release and oxidative stress pathways, illustrating that long-term accumulation of even “eco-friendly” nanomaterials can extend toxicological footprints beyond initial remediation goals if not carefully controlled and assessed (Ferdush et al., 2025).

11. Conclusion

Agriculturally derived nanomaterials represent a rapidly advancing, up-and-coming class of bio-derived technologies with the capacity to transform disease prevention across multiple sectors. Their unique combination of nanoscale properties, inherent bioactivity, sustainability, and biocompatibility positions them at the frontier of innovative solutions for plant protection, animal health, human medicine, food safety, and environmental remediation. Through green, resource-efficient synthesis pathways, these nanomaterials offer multifunctional capabilities, ranging from antimicrobial and immunomodulatory activities to targeted delivery of therapeutic and nutraceutical agents, collectively supporting integrated One Health approaches. Despite significant progress, several limitations impede the full-scale implementation of agriculturally sourced nanomaterials. Variability in biomass composition, challenges in synthesis standardization, concerns regarding long-term safety, and the absence of cohesive regulatory frameworks remain critical barriers. Addressing these gaps requires coordinated efforts in mechanistic research, toxicological studies, industrial-scale process development, and policy harmonization. The incorporation of emerging technologies, such as artificial intelligence, advanced characterization tools, and systems-level modelling, will be essential for guiding rational design and ensuring safe and effective deployment. Looking forward, agriculturally based nanomaterials offer transformative potential to advance global goals in health security, sustainable agriculture, food system resilience, and environmental quality.

9. Gaps and Limitations

Agriculturally derived nanomaterials offer multiple opportunities for sustainable and effective disease prevention across plant, animal, human, and environmental health domains. They utilize renewable resources, such as plant extracts, agricultural waste, and natural biopolymers, reducing dependence on non-renewable chemical precursors. Their synthesis typically involves low-toxicity reagents, minimal energy consumption, and reduced environmental footprint, aligning with green chemistry principles. Consequently, among other advantages, by enhancing efficiency and providing natural antimicrobial alternatives, agriculturally based nanomaterials can lower the need for chemical pesticides, synthetic fertilizers, and antibiotics. This reduction supports environmental health and mitigates concerns about antimicrobial resistance (AMR). However, despite their promising attributes, several limitations constrain their widespread adoption and translational scalability. Among them is their greater variation across plant type, environmental conditions, growth stage, and extraction methods. This variability impacts nanoparticle morphology, size distribution, surface chemistry, and reproducibility, thereby making standardization difficult. Also, long-term studies on exposure, biodegradation pathways, accumulation in food chains, and ecosystem impacts are scarce. The absence of robust data complicates risk assessment and raises concerns about unintended consequences. Therefore, given the significant opportunities offered by agriculturally based nanomaterials, their deployment must be guided by scientific evidence, careful risk assessment, and standardization.

10. Future Work

Future work should focus on refining biogenic synthesis methods to achieve greater control over nanoparticle size, shape, surface chemistry, and reproducibility. These improvements will help bridge the gap between laboratory synthesis and industrial-scale production. Furthermore, these findings underscore the need for comprehensive life-cycle assessments, environmental fate studies, and dose-response toxicological evaluations to balance the technological advantages of ABNMs with environmental and health safety considerations. Attention should be given to long-term ecotoxicological investigations, multi-generational exposure assessments in plants and animals, evaluation of nanoparticle accumulation and biodegradation pathways, and the development of predictive models for environmental fate and transport. Also, collaboration is essential to develop harmonized international standards for biogenic nanomaterials, establish guidelines for labelling, risk communication, and quality control, create regulatory pathways tailored to nanoscale products of biological origin, and promote transparent reporting and data-sharing frameworks. These measures will help build public trust and streamline commercialization.

Disclaimer (Artificial Intelligence)

Author(s) hereby declares that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc) and text-to-image generators have been used during the writing or editing of this manuscript.

Competing interests

Authors have declared that no competing interests exist.

COMPETING INTERESTS DISCLAIMER:

Authors have declared that they have no known competing financial interests OR non-financial interests OR personal relationships that could have appeared to influence the work reported in this paper.

References

- Abbasi, A. M., Shah, M. H., & Khan, M. A. (2014). Phytochemicals and nutraceuticals. In Wild Edible Vegetables of Lesser Himalayas: Ethnobotanical and Nutraceutical Aspects, Volume 1 (pp. 31–65). Springer.

- Acharya, C., Mishra, S., Chaurasia, S. K., Pandey, B. K., Dhar, R., & Pandey, J. K. (2025). Synthesis of metallic nanoparticles using biometabolites: mechanisms and applications. BioMetals, 38(1), 21–54.

- Adetunji, C. O., Olaniyan, O. T., Anani, O. A., Olisaka, F. N., Inobeme, A., Bodunrinde, R. E., Adetunji, J. B., Singh, K. R., Palnam, W. D., & Singh, R. P. (2021). Current scenario of nanomaterials in the environmental, agricultural, and biomedical fields. In Nanomaterials in Bionanotechnology (pp. 129–158). CRC Press.

- Agarwalla, A., Ahmed, W., Al-Marzouqi, A. H., Rizvi, T. A., Khan, M., & Zaneldin, E. (2023). Characteristics and key features of antimicrobial materials and associated mechanisms for diverse applications. Molecules, 28(24), 8041.

- Ahmed, H. M., Roy, A., Wahab, M., Ahmed, M., Othman-Qadir, G., Elesawy, B. H., Khandaker, M. U., Islam, M. N., & Emran, T. B. (2021). Applications of nanomaterials in agrifood and pharmaceutical industry. Journal of Nanomaterials, 2021(1), 1472096.

- Akande, O. W., & Akande, T. M. (2020). COVID-19 pandemic: A global health burden. Nigerian Postgraduate Medical Journal, 27(3), 147–155.

- Al Hunaiti, A., Hamideh, M., & Al-Shawabkeh, R. (2025). Magnetic nanoparticles of TiO2-NiFe2O4-Chitosan for photocatalytic degradation: synthesis, characterization, methyl blue dye-VOCs wastewater treatment, kinetic experimental, and theoretical studies. Emergent Materials, 8(1), 45–60.

- Ali, J., Ali, N., Wang, L., Waseem, H., & Pan, G. (2019). Revisiting the mechanistic pathways for bacterial mediated synthesis of noble metal nanoparticles. Journal of Microbiological Methods, 159, 18–25.

- Amendola, V., & Meneghetti, M. (2009). Laser ablation synthesis in solution and size manipulation of noble metal nanoparticles. Physical chemistry chemical physics, 11(20), 3805–3821.

- Anupong, W., On-Uma, R., Jutamas, K., Joshi, D., Salmen, S. H., Alahmadi, T. A., & Jhanani, G. (2023). Cobalt nanoparticles synthesizing potential of orange peel aqueous extract and their antimicrobial and antioxidant activity. Environmental Research, 216, 114594.

- Ashbolt, N. J. (2004). Microbial contamination of drinking water and disease outcomes in developing regions. Toxicology, 198(1-3), 229–238.

- Ashour, B., Ali, S. M., Farahat, M. G., & El‑Sherif, R. M. (2025). Fabrication and Detection of Carbon-based Nanomaterials Derived from Biomass Sources: Processes and Applications. Egyptian Journal of Chemistry, 68(7), 117–129.

- Aslam, R., Wang, Q., Aslam, A., & Yan, Z. (2025). Methods Used to Convert Waste Material into Carbon Nanomaterials. Waste Derived Carbon Nanomaterials. Volume 1, 71–94.

- Aswini, R., Jothimani, K., Kannan, K., Pothu, R., Shanmugam, P., Boddula, R., Radwan, A. B., Periyasami, G., Karthikeyan, P., & Al-Qahtani, N. (2024). Carica Papaya leaf-infused metal oxide nanocomposite: a green approach towards water treatment and antibacterial applications. Environmental Geochemistry and Health, 46(9), 334.

- Avitabile, E., Senes, N., D’avino, C., Tsamesidis, I., Pinna, A., Medici, S., & Pantaleo, A. (2020). The potential antimalarial efficacy of hemocompatible silver nanoparticles from Artemisia species against P. falciparum parasite. PloS one, 15(9), e0238532.

- Banerjee, K., Madhyastha, R., Nakajima, Y., Maruyama, M., & Madhyastha, H. (2021). Nanoceutical adjuvants as wound healing material: precepts and prospects. International journal of molecular sciences, 22(9), 4748.

- Banik, A., & Basu, S. (2025). Drivers and Consequences of Viral Zoonoses: Public Health and Economic Perspectives. Zoonotic Diseases, 5(4), 32.

- Barhoum, A., Jeevanandam, J., Rastogi, A., Samyn, P., Boluk, Y., Dufresne, A., Danquah, M. K., & Bechelany, M. (2020). Plant celluloses, hemicelluloses, lignins, and volatile oils for the synthesis of nanoparticles and nanostructured materials. Nanoscale, 12(45), 22845–22890.

- Baweja, P., Kumar, S., & Kumar, G. (2020). Fertilizers and pesticides: Their impact on soil health and environment. In Soil health (pp. 265–285). Springer.

- Bekah, D., Boyjoo, Y., Panpadoo, R. M., White, J. C., & Bhaw-Luximon, A. (2025). Nanostimulants and nanofertilizers for precision agriculture: transforming food production in the 21st century. Environmental Science: Nano.

- Benatar, S. R., Gill, S., & Bakker, I. (2013). Global health and the global economic crisis. In Health and human rights in a changing world (pp. 487–500). Routledge.

- Bentrad, N. (2025). Nanotoxicology and Environmental Health Impacts. In Advances in Nanomaterials for Detection, Control, and Removal of Environmental Pollutants (pp. 171–196). Springer.

- Bhargava, P. C., Kamal, N., Chaurasia, D., Singh, S., & Singh, A. (2024). 14 Agro-Residues’ Waste. Waste-to-Wealth: Resource Recovery and Value-Added Products for Sustainable Development, 200.

- Brinchi, L., Cotana, F., Fortunati, E., & Kenny, J. M. (2013). Production of nanocrystalline cellulose from lignocellulosic biomass: technology and applications. Carbohydrate polymers, 94(1), 154–169.

- Calvo, P., Remunan‐Lopez, C., Vila‐Jato, J. L., & Alonso, M. (1997). Novel hydrophilic chitosan‐polyethylene oxide nanoparticles as protein carriers. Journal of applied polymer science, 63(1), 125–132.

- Chakroborty, S., Pal, K., Nath, N., Singh, V., Barik, A., Soren, S., Panda, P., Asthana, N., & Kyzas, G. Z. (2023). Sustainable synthesis of multifunctional nanomaterials from rice wastes: a comprehensive review. Environmental Science and Pollution Research, 30(42), 95039–95053.

- Chand, S., Kumar, R., & Kumar, K. (2025). Plant Waste-Derived Carbon Nanomaterials. In Waste Derived Carbon Nanomaterials. Volume 1 (pp. 115–148). ACS Publications.

- Chang, C., Wang, T., Hu, Q., & Luo, Y. (2017). Caseinate-zein-polysaccharide complex nanoparticles as potential oral delivery vehicles for curcumin: Effect of polysaccharide type and chemical cross-linking. Food Hydrocolloids, 72, 254–262.

- Chen, X., Chen, H., Zhang, H., Peng, Y., Deng, F., Gao, J., Chai, C., Tang, S., Zuo, X., & Lu, J. (2019). Characterization of synergistic antibacterial effect of silver nanoparticles and ebselen. Artificial cells, nanomedicine, and biotechnology, 47(1), 3338–3349.

- Cozzoli, P. D., & Manna, L. (2007). Synthetic strategies to size and shape controlled nanocrystals and nanocrystal heterostructures. Bio-Applications of Nanoparticles, 1–17.

- De Yoreo, J. J. (2010). Physical mechanisms of crystal growth modification by biomolecules. AIP Conference Proceedings,

- Devi, M. S., Thangadurai, T. D., Shanmugaraju, S., Selvan, C. P., & Lee, Y. I. (2024). Biomass waste from walnut shell for pollutants removal and energy storage: a review on waste to wealth transformation. Adsorption, 30(6), 891–913.

- Díez-Pascual, A. M. (2020). Recent progress in antimicrobial nanomaterials. Nanomaterials, 10(11), 2315.

- Dilshad, E., Bibi, M., Sheikh, N. A., Tamrin, K. F., Mansoor, Q., Maqbool, Q., & Nawaz, M. (2020). Synthesis of functional silver nanoparticles and microparticles with modifiers and evaluation of their antimicrobial, anticancer, and antioxidant activity. Journal of functional biomaterials, 11(4), 76.

- Dong, B.-R., Jiang, R., Chen, J.-F., Xiao, Y., Lv, Z.-Y., & Chen, W.-S. (2023). Strategic nanoparticle-mediated plant disease resistance. Critical Reviews in Biotechnology, 43(1), 22–37.

- El-Hussein, A., Mounir, M., El-Sayed, M. A., & Abd El-sadek, M. (2024). Green synthesis of nano materials and their applications. In Comprehensive Analytical Chemistry (Vol. 105, pp. 461–491). Elsevier.

- El-Kattan, N., Emam, A. N., Mansour, A. S., Ibrahim, M. A., Abd El-Razik, A. B., Allam, K. A., Riad, N. Y., & Ibrahim, S. A. (2022). Curcumin assisted green synthesis of silver and zinc oxide nanostructures and their antibacterial activity against some clinical pathogenic multi-drug resistant bacteria. RSC advances, 12(28), 18022–18038.

- Elshafie, H. S., Camele, I., & Mohamed, A. A. (2023). A comprehensive review on the biological, agricultural and pharmaceutical properties of secondary metabolites based-plant origin. International journal of molecular sciences, 24(4), 3266.

- Endale, H., Mathewos, M., & Abdeta, D. (2023). Potential causes of spread of antimicrobial resistance and preventive measures in one health perspective-a review. Infection and drug resistance, 7515–7545.

- Erofeeva, E. A. (2025). Hormesis and Nanomaterials. From Biostimulation to Toxicity. In Plant Biostimulation with Nanomaterials (pp. 1–19). Springer.

- Farid, A. (2025). Herbal Pharmacopeia: Nanotechnology and Advancing Drug Discovery. CRC Press.

- Farringtonargue, J. (2012). AFRICA’S NEXT BURDEN Non-infectious disease. BMJ, 345, 25.

- Ferdush, J., Rahman, M. M., Parvez, M. M. H., Mohotadi, M. A. A., & Uddin, M. N. (2025). Green-Synthesized Nanomaterials for Water Disinfection: Mechanisms, Efficacy, and Environmental Safety. Nanomaterials, 15(19), 1507.

- Filip, R., Gheorghita Puscaselu, R., Anchidin-Norocel, L., Dimian, M., & Savage, W. K. (2022). Global challenges to public health care systems during the COVID-19 pandemic: a review of pandemic measures and problems. Journal of personalized medicine, 12(8), 1295.

- Fu, L., Wang, Z., Dhankher, O. P., & Xing, B. (2020). Nanotechnology as a new sustainable approach for controlling crop diseases and increasing agricultural production. Journal of Experimental Botany, 71(2), 507–519.

- Gamelas, J. A., Pedrosa, J., Lourenço, A. F., Mutjé, P., González, I., Chinga-Carrasco, G., Singh, G., & Ferreira, P. J. (2015). On the morphology of cellulose nanofibrils obtained by TEMPO-mediated oxidation and mechanical treatment. Micron, 72, 28–33.

- Gandhi, P. R., Jayaseelan, C., Kamaraj, C., Rajasree, S. R., & Mary, R. R. (2018). In vitro antimalarial activity of synthesized TiO2 nanoparticles using Momordica charantia leaf extract against Plasmodium falciparum. Journal of Applied Biomedicine, 16(4), 378–386.

- Gebre, S. H. (2023). Bio-inspired synthesis of metal and metal oxide nanoparticles: the key role of phytochemicals. Journal of Cluster Science, 34(2), 665–704.

- Gourama, H. (2020). Foodborne pathogens. In Food safety engineering (pp. 25–49). Springer.

- Guerrini, L., Alvarez-Puebla, R. A., & Pazos-Perez, N. (2018). Surface modifications of nanoparticles for stability in biological fluids. Materials, 11(7), 1154.

- Gupta, S., Choudhary, D. K., & Sundaram, S. (2025). Green synthesis and characterization of silver nanoparticles using Citrus sinensis (Orange peel) extract and their antidiabetic, antioxidant, antimicrobial and anticancer activity. Waste and Biomass Valorization, 16(3), 1101–1114.

- Habibi, Y., Lucia, L. A., & Rojas, O. J. (2010). Cellulose nanocrystals: chemistry, self-assembly, and applications. Chemical reviews, 110(6), 3479–3500.

- Hachem, K., Ansari, M. J., Saleh, R. O., Kzar, H. H., Al-Gazally, M. E., Altimari, U. S., Hussein, S. A., Mohammed, H. T., Hammid, A. T., & Kianfar, E. (2022). Methods of chemical synthesis in the synthesis of nanomaterial and nanoparticles by the chemical deposition method: a review. BioNanoScience, 12(3), 1032–1057.

- Harish, V., Tewari, D., Gaur, M., Yadav, A. B., Swaroop, S., Bechelany, M., & Barhoum, A. (2022). Review on nanoparticles and nanostructured materials: Bioimaging, biosensing, drug delivery, tissue engineering, antimicrobial, and agro-food applications. Nanomaterials, 12(3), 457.

- Hassan Afandy, H., Sabir, D. K., & Aziz, S. B. (2023). Antibacterial activity of the green synthesized plasmonic silver nanoparticles with crystalline structure against gram-positive and gram-negative bacteria. Nanomaterials, 13(8), 1327.

- Hayat, M., Rehman, A., Khan, F. A., Anees, M., Naz, I., Qasim, M., & Kanwal, N. (2024). Phytogenic-mediated zinc oxide nanoparticles using the seed extract of Citrullus lanatus and its integrated potency against multidrug resistant bacteria. ACS omega, 9(14), 16832–16841.

- Hazards, E. P. o. B., Koutsoumanis, K., Allende, A., Álvarez‐Ordóñez, A., Bolton, D., Bover‐Cid, S., Chemaly, M., Davies, R., De Cesare, A., & Herman, L. (2021). Role played by the environment in the emergence and spread of antimicrobial resistance (AMR) through the food chain. Efsa Journal, 19(6), e06651.

- Hönig, M., Roeber, V. M., Schmülling, T., & Cortleven, A. (2023). Chemical priming of plant defense responses to pathogen attacks. Frontiers in plant science, 14, 1146577.

- Howard, D., Sebastian, S., Le, Q. V.-C., Thierry, B., & Kempson, I. (2020). Chemical mechanisms of nanoparticle radiosensitization and radioprotection: a review of structure-function relationships influencing reactive oxygen species. International journal of molecular sciences, 21(2), 579.

- Hulkoti, N. I., & Taranath, T. (2014). Biosynthesis of nanoparticles using microbes—a review. Colloids and surfaces B: Biointerfaces, 121, 474–483.

- Hussien, N. A. (2023). Antimicrobial potential of biosynthesized zinc oxide nanoparticles using banana peel and date seeds extracts. Sustainability, 15(11), 9048.

- Iavicoli, I., Leso, V., Fontana, L., & Calabrese, E. J. (2018). Nanoparticle exposure and hormetic dose–responses: An update. International journal of molecular sciences, 19(3), 805.

- Ibrahim, H. M. (2015). Green synthesis and characterization of silver nanoparticles using banana peel extract and their antimicrobial activity against representative microorganisms. Journal of radiation research and applied sciences, 8(3), 265–275.

- Iqbal, A., Hafeez, S., Bibi, S., & Narasimharao, K. (2026). Fabrication strategies and properties of green and sustainable nanomaterials. In Sustainable Green Nanomaterials for Mitigation of Microplastics and Plastic Additives Pollution (pp. 1–35). Elsevier.

- Iravani, S., & Varma, R. S. (2020). Bacteria in heavy metal remediation and nanoparticle biosynthesis. ACS Sustainable Chemistry & Engineering, 8(14), 5395–5409.

- Isogai, A. (2020). Cellulose nanofibers: recent progress and future prospects. Journal of Fiber Science and Technology, 76(10), 310–326.

- Isogai, A., Saito, T., & Fukuzumi, H. (2011). TEMPO-oxidized cellulose nanofibers. Nanoscale, 3(1), 71–85.

- Jacob, R. H., Afify, A. S., Shanab, S. M., & Shalaby, E. A. (2024). Chelated amino acids: biomass sources, preparation, properties, and biological activities. Biomass Conversion and Biorefinery, 14(3), 2907–2921.

- Javaid, A., Hameed, S., Li, L., Zhang, Z., Zhang, B., & -Rahman, M.-u. (2024). Can nanotechnology and genomics innovations trigger agricultural revolution and sustainable development? Functional & Integrative Genomics, 24(6), 216.

- Javed, R., Zia, M., Naz, S., Aisida, S. O., Ain, N. u., & Ao, Q. (2020). Role of capping agents in the application of nanoparticles in biomedicine and environmental remediation: recent trends and future prospects. Journal of Nanobiotechnology, 18(1), 172.

- John, K. I., Adeleye, A. T., Munsif, S., Odusina, B. O., & Omorogie, M. O. (2025). Perspectives on Circular Economy and Efficient Resource Utilization of Valorized Value-Added Material for Sustainable Development.

- Joseph, S. (2015). Biochar for environmental management: science, technology and implementation. Routledge.

- Karnwal, A., Sharma, V., Kumar, G., Jassim, A. Y., Dohroo, A., & Sivanesan, I. (2024). Transforming medicine with nanobiotechnology: nanocarriers and their biomedical applications. Pharmaceutics, 16(9), 1114.

- Kaur, H., Kumar, S., & Bouzid, G. (2024). Exploring the role of different phytochemicals on the morphological variations of metal and metal oxide nanomaterials for biomedical application. Interactions, 245(1), 234.

- Kheiriabad, S., Jafari, A., Namvar Aghdash, S., Ezzati Nazhad Dolatabadi, J., Andishmand, H., & Jafari, S. M. (2024). Applications of advanced nanomaterials in biomedicine, pharmaceuticals, agriculture, and food industry. BioNanoScience, 14(4), 4298–4321.

- Klemm, D., Kramer, F., Moritz, S., Lindström, T., Ankerfors, M., Gray, D., & Dorris, A. (2011). Nanocelluloses: a new family of nature‐based materials. Angewandte Chemie International Edition, 50(24), 5438–5466.

- Kumar, H., Bhardwaj, K., Sharma, R., Nepovimova, E., Kuča, K., Dhanjal, D. S., Verma, R., Bhardwaj, P., Sharma, S., & Kumar, D. (2020). Fruit and vegetable peels: utilization of high value horticultural waste in novel industrial applications. Molecules, 25(12), 2812.

- Kuppusamy, P., Yusoff, M. M., Maniam, G. P., & Govindan, N. (2016). Biosynthesis of metallic nanoparticles using plant derivatives and their new avenues in pharmacological applications–An updated report. Saudi Pharmaceutical Journal, 24(4), 473–484.

- Li, B., Xu, W., Kronlund, D., Määttänen, A., Liu, J., Smått, J.-H., Peltonen, J., Willför, S., Mu, X., & Xu, C. (2015). Cellulose nanocrystals prepared via formic acid hydrolysis followed by TEMPO-mediated oxidation. Carbohydrate polymers, 133, 605–612.

- Li, C., He, W., Cui, Y., Wu, S., Song, Q. a., Li, Y., Guo, J., Ge, X., & Tian, P. (2025). Dual-functional berberine-magnolol co-assembled nanoparticles inhibit Fusarium graminearum growth and mycotoxin production. Pesticide Biochemistry and Physiology, 106523.

- Li, Y., Zhang, P., Li, M., Shakoor, N., Adeel, M., Zhou, P., Guo, M., Jiang, Y., Zhao, W., & Lou, B. (2023). Application and mechanisms of metal‐based nanoparticles in the control of bacterial and fungal crop diseases. Pest Management Science, 79(1), 21–36.

- Lin, X., Yu, W., Tong, X., Li, C., Duan, N., Wang, Z., & Wu, S. (2024). Application of nanomaterials for coping with mycotoxin contamination in food safety: from detection to control. Critical Reviews in Analytical Chemistry, 54(2), 355–388.

- Liu, J., Liu, Z., Pang, Y., & Zhou, H. (2022). The interaction between nanoparticles and immune system: application in the treatment of inflammatory diseases. Journal of Nanobiotechnology, 20(1), 127.

- Lizundia, E., Sipponen, M. H., Greca, L. G., Balakshin, M., Tardy, B. L., Rojas, O. J., & Puglia, D. (2021). Multifunctional lignin-based nanocomposites and nanohybrids. Green Chemistry, 23(18), 6698–6760.

- Mackenzie, J., Childs, J., & Richt, J. (2007). The Biology, Circumstances and Consequences of Cross-Species Transmission. Springer.

- Magouras, I., Brookes, V. J., Jori, F., Martin, A., Pfeiffer, D. U., & Dürr, S. (2020). Emerging zoonotic diseases: should we rethink the animal–human interface? Frontiers in Veterinary Science, 7, 582743.

- Makofane, A., Motaung, D. E., & Hintsho-Mbita, N. C. (2021). Photocatalytic degradation of methylene blue and sulfisoxazole from water using biosynthesized zinc ferrite nanoparticles. Ceramics International, 47(16), 22615–22626.

- Manjari, G., Parthiban, A., & Saran, S. (2020). Sustainable utilization of molasses towards green synthesis of silver nanoparticles for colorimetric heavy metal sensing and catalytic applications. Journal of Cluster Science, 31(5), 1137–1145.

- Mannaa, M., & Kim, K. D. (2017). Influence of temperature and water activity on deleterious fungi and mycotoxin production during grain storage. Mycobiology, 45(4), 240–254.

- Mba, I. E., & Nweze, E. I. (2022). Antimicrobial peptides therapy: an emerging alternative for treating drug-resistant bacteria. The Yale journal of biology and medicine, 95(4), 445.

- Meena, M., Swapnil, P., Barupal, T., & Sharma, K. (2019). A review on infectious pathogens and mode of transmission. J. Plant Pathol. Microbiol, 10, 472.

- Miller, K. P., Wang, L., Benicewicz, B. C., & Decho, A. W. (2015). Inorganic nanoparticles engineered to attack bacteria. Chemical Society Reviews, 44(21), 7787–7807.

- Mmbando, G. S., Ally, O., & Kitimu, S. R. (2025). The current use of nanotechnology in the fight against antimicrobial resistance: promising approaches to global health challenge. Journal of Nanoparticle Research, 27(4), 1–19.

- Modi, S. K., Gaur, S., Sengupta, M., & Singh, M. S. (2023). Mechanistic insights into nanoparticle surface-bacterial membrane interactions in overcoming antibiotic resistance. Frontiers in microbiology, 14, 1135579.

- Mohammed, K. S., Atlabachew, M., Abdu, B., & Desalew, A. A. (2024). A nanocellulose from sugarcane bagasse as a template for nickel oxide nanoparticles for removal of organic dyes from aqueous solution. Scientific Reports, 14(1), 31684.

- Murugan, S., Senthilvelan, T., Govindasamy, M., & Thangavel, K. (2025). A Comprehensive Review on Exploring the Potential of Phytochemicals and Biogenic Nanoparticles for the Treatment of Antimicrobial-Resistant Pathogenic Bacteria. Current Microbiology, 82(2), 90.

- Narayanan, K. B., & Sakthivel, N. (2010). Biological synthesis of metal nanoparticles by microbes. Advances in colloid and interface science, 156(1-2), 1–13.

- Nasrollahzadeh, M., Mahmoudi‐Gom Yek, S., Motahharifar, N., & Ghafori Gorab, M. (2019). Recent developments in the plant‐mediated green synthesis of Ag‐based nanoparticles for environmental and catalytic applications. The Chemical Record, 19(12), 2436–2479.

- Nath, P. C., Ojha, A., Debnath, S., Sharma, M., Sridhar, K., Nayak, P. K., & Inbaraj, B. S. (2023). Biogeneration of valuable nanomaterials from agro-wastes: A comprehensive review. Agronomy, 13(2), 561.

- Nechyporchuk, O., Belgacem, M. N., & Bras, J. (2016). Production of cellulose nanofibrils: A review of recent advances. Industrial Crops and Products, 93, 2–25.

- Nguyen, V. T. (2017). Potential, uses and future perspectives of agricultural wastes. Recovering bioactive compounds from agricultural wastes, 1–32.

- Nobahar, A., Carlier, J. D., Miguel, M. G., & Costa, M. C. (2021). A review of plant metabolites with metal interaction capacity: a green approach for industrial applications. BioMetals, 34(4), 761–793.

- Okus, F., Yuzbasioglu, D., & Unal, F. (2025). Green synthesized metal nanoparticles appear to meet expectations of low ecotoxicity: what about genotoxicity? Toxicology Mechanisms and Methods, 1–15.

- Okuthe, G. E., & Siguba, B. (2025). Acute Dermatotoxicity of Green-Synthesized Silver Nanoparticles (AgNPs) in Zebrafish Epidermis. Toxics, 13(7), 592.

- Oladunjoye, I. O., Tajudeen, Y. A., Oladipo, H. J., & El-Sherbini, M. S. (2022). Planetary health and traditional medicine: a potential synergistic approach to tackle antimicrobial resistance. Challenges, 13(1), 24.

- Ovais, M., Khalil, A. T., Islam, N. U., Ahmad, I., Ayaz, M., Saravanan, M., Shinwari, Z. K., & Mukherjee, S. (2018). Role of plant phytochemicals and microbial enzymes in biosynthesis of metallic nanoparticles. Applied microbiology and biotechnology, 102(16), 6799–6814.

- Pääkkö, M., Ankerfors, M., Kosonen, H., Nykänen, A., Ahola, S., Österberg, M., Ruokolainen, J., Laine, J., Larsson, P. T., & Ikkala, O. (2007). Enzymatic hydrolysis combined with mechanical shearing and high-pressure homogenization for nanoscale cellulose fibrils and strong gels. Biomacromolecules, 8(6), 1934–1941.

- Pathakoti, K., Goodla, L., Manubolu, M., & Hwang, H.-M. (2019). Nanoparticles and their potential applications in agriculture, biological therapies, food, biomedical, and pharmaceutical industry: a review. Nanotechnology and nanomaterial applications in food, health, and biomedical sciences, 121–162.

- Patra, J. K., Shin, H.-S., Yang, I.-J., Nguyen, L. T. H., & Das, G. (2024). Sustainable utilization of food biowaste (papaya peel) extract for gold nanoparticle biosynthesis and investigation of its multi-functional potentials. Antioxidants, 13(5), 581.

- Paul, J. (2024). Introduction to infectious diseases. In Disease Causing Microbes (pp. 1–63). Springer.

- Plucinski, A., Lyu, Z., & Schmidt, B. V. (2021). Polysaccharide nanoparticles: from fabrication to applications. Journal of Materials Chemistry B, 9(35), 7030–7062.

- Priya, A., Alagumalai, A., Balaji, D., & Song, H. (2023). Bio-based agricultural products: a sustainable alternative to agrochemicals for promoting a circular economy. RSC Sustainability, 1(4), 746–762.

- Rahman, S., Sadaf, S., Hoque, M. E., Mishra, A., Mubarak, N. M., Malafaia, G., & Singh, J. (2024). Unleashing the promise of emerging nanomaterials as a sustainable platform to mitigate antimicrobial resistance. RSC advances, 14(20), 13862–13899.

- Rajput, V. D., Minkina, T., Sushkova, S., Tsitsuashvili, V., Mandzhieva, S., Gorovtsov, A., Nevidomskyaya, D., & Gromakova, N. (2018). Effect of nanoparticles on crops and soil microbial communities. Journal of Soils and Sediments, 18(6), 2179–2187.

- Ranganathan, S., Dutta, S., Moses, J., & Anandharamakrishnan, C. (2020). Utilization of food waste streams for the production of biopolymers. Heliyon, 6(9).

- Rath, S. (2021). Microbial contamination of drinking water. In Water Pollution and Management Practices (pp. 1–17). Springer.

- Rawal, K., & Acharya, M. A. (2024). TOWARDS SUSTAINABLE HEALTHCARE: NAVIGATING INNOVATIVE PRACTICES FOR ADAPTATION AND IMPACT. Interdisciplinary Perspectives on Sustainable Development from Vision to Action.

- Rich, K. M., & Perry, B. D. (2011). The economic and poverty impacts of animal diseases in developing countries: new roles, new demands for economics and epidemiology. Preventive veterinary medicine, 101(3-4), 133–147.

- Rigopoulos, N., Thomou, E., Kouloumpis, A., Lamprou, E. R., Petropoulea, V., Gournis, D., Poulios, E., Karantonis, H. C., & Giaouris, E. (2019). Optimization of silver nanoparticle synthesis by banana peel extract using statistical experimental design, and testing of their antibacterial and antioxidant properties. Current pharmaceutical biotechnology, 20(10), 858–873.

- Rinaudo, M. (2006). Chitin and chitosan: Properties and applications. Progress in polymer science, 31(7), 603–632.

- Rohaizu, R., & Wanrosli, W. (2017). Sono-assisted TEMPO oxidation of oil palm lignocellulosic biomass for isolation of nanocrystalline cellulose. Ultrasonics Sonochemistry, 34, 631–639.

- Rotimi, L., Ojemaye, M. O., Okoh, O. O., Sadimenko, A., & Okoh, A. I. (2019). Synthesis, characterization, antimalarial, antitrypanocidal and antimicrobial properties of gold nanoparticle. Green Chemistry Letters and Reviews, 12(1), 61–68.

- Roy, A., Roy, M., Alghamdi, S., Dablool, A. S., Almakki, A. A., Ali, I. H., Yadav, K. K., Islam, M. R., & Cabral-Pinto, M. M. (2022). Role of microbes and nanomaterials in the removal of pesticides from wastewater. International Journal of Photoenergy, 2022(1), 2131583.

- Ruangtong, J., Jiraroj, T., & T-Thienprasert, N. P. (2020). Green synthesized ZnO nanosheets from banana peel extract possess anti-bacterial activity and anti-cancer activity. Materials Today Communications, 24, 101224.

- Salem, S. S., Badawy, M. S. E., Al-Askar, A. A., Arishi, A. A., Elkady, F. M., & Hashem, A. H. (2022). Green biosynthesis of selenium nanoparticles using orange peel waste: Characterization, antibacterial and antibiofilm activities against multidrug-resistant bacteria. Life, 12(6), 893.

- Saod, W. M., Hamid, L. L., Alaallah, N. J., & Ramizy, A. (2022). Biosynthesis and antibacterial activity of manganese oxide nanoparticles prepared by green tea extract. Biotechnology Reports, 34, e00729.

- Sevilla, M., & Fuertes, A. B. (2009). The production of carbon materials by hydrothermal carbonization of cellulose. Carbon, 47(9), 2281–2289.

- Shaji, S., Jose, J., Jose, J., Jose, J., & Distante, A. (2025). Wound Healing and Controlled Drug Release Using the Synergistic Role of Bionanocomposites. Advanced Bionanocomposite Materials: Innovations for Sustainable Development, 221–246.

- Sharmin, S., Rahaman, M. M., Sarkar, C., Atolani, O., Islam, M. T., & Adeyemi, O. S. (2021). Nanoparticles as antimicrobial and antiviral agents: A literature-based perspective study. Heliyon, 7(3).

- Singh, J., Kumar, A., Nayal, A. S., Vikal, S., Shukla, G., Singh, A., Singh, A., Goswami, S., Kumar, A., & Gautam, Y. K. (2024). Comprehensive antifungal investigation of green synthesized silver nanoformulation against four agriculturally significant fungi and its cytotoxic applications. Scientific Reports, 14(1), 5934.

- Siró, I., & Plackett, D. (2010). Microfibrillated cellulose and new nanocomposite materials: a review. Cellulose, 17(3), 459–494.

- Smith, K. M., Machalaba, C. C., Seifman, R., Feferholtz, Y., & Karesh, W. B. (2019). Infectious disease and economics: The case for considering multi-sectoral impacts. One health, 7, 100080.

- Suhag, R., Kumar, R., Dhiman, A., Sharma, A., Prabhakar, P. K., Gopalakrishnan, K., Kumar, R., & Singh, A. (2023). Fruit peel bioactives, valorisation into nanoparticles and potential applications: A review. Critical Reviews in Food Science and Nutrition, 63(24), 6757–6776.

- Tarbali, S., Karami Mehrian, S., & Khezri, S. (2022). Toxicity effects evaluation of green synthesized silver nanoparticles on intraperitoneally exposed male Wistar rats. Toxicology Mechanisms and Methods, 32(7), 488–500.

- Thanh, N. T., Maclean, N., & Mahiddine, S. (2014). Mechanisms of nucleation and growth of nanoparticles in solution. Chemical reviews, 114(15), 7610–7630.

- Titirici, M.-M., & Antonietti, M. (2010). Chemistry and materials options of sustainable carbon materials made by hydrothermal carbonization. Chemical Society Reviews, 39(1), 103–116.

- Tiwari, S., Kumar, R., Devi, S., Sharma, P., Chaudhary, N. R., Negi, S., Tandel, N., Marepally, S., Pied, S., & Tyagi, R. K. (2024). Biogenically synthesized green silver nanoparticles exhibit antimalarial activity. Discover nano, 19(1), 136.

- Tohamy, H.-A., El-Sakhawy, M., & Kamel, S. (2025). A greener future: carbon nanomaterials from lignocellulose. Journal of Renewable Materials, 13(1), 21.

- Törős, G., Gulyás, G., El-Ramady, H., Alibrahem, W., Muthu, A., Gangakhedkar, P., Atieh, R., & Prokisch, J. (2025). Sustainable Nanotechnology Strategies for Modulating the Human Gut Microbiota. International journal of molecular sciences, 26(12), 5433.

- Tyagi, P. K., Gupta, S., Tyagi, S., Kumar, M., Pandiselvam, R., Daştan, S. D., Sharifi-Rad, J., Gola, D., & Arya, A. (2021). Green synthesis of iron nanoparticles from spinach leaf and banana peel aqueous extracts and evaluation of antibacterial potential. Journal of Nanomaterials, 2021(1), 4871453.

- Ul-Hamid, A., Baig, N., Haider, A., Hakeem, A. S., & Ikram, M. (2023). Using biologically synthesized TiO2 nanoparticles as potential remedy against multiple drug resistant Staphylococcus aureus of bovine mastitis. Scientific Reports, 13(1), 18785.

- Vasile, C., Tantaru, G., & Creteanu, A. (2025). Recent Insights into the Research of (Bio) Active Additives for Advanced Polymer Materials. Polymers, 17(23), 3139.

- Veeragoni, D., Deshpande, S. S., Singh, V., Misra, S., & Mutheneni, S. R. (2023). In vitro and in vivo antimalarial activity of green synthesized silver nanoparticles using Sargassum tenerrimum-a marine seaweed. Acta Tropica, 245, 106982.

- Verma, R., Dutta, S., Kumar, A., Dabodiya, T. S., Kumar, N., Karuppasamy, K. S. K., Sangmesh, B., Jaiswal, A., & Jaiswal, K. K. (2023). Biochar-Based nanocomposite materials: types, characteristics, physical activation, and diverse application scenarios. In Biochar-Based Nanocomposites for Contaminant Management: Synthesis, Contaminants Removal, and Environmental Sustainability (pp. 3–18). Springer.

- Verma, V., Gupta, P., Singh, P., & Pandey, N. K. (2025). Biomaterials and Their Fabrication for Advanced Bionanocomposites: A Sustainable Approach. In Advanced Bionanocomposite Materials: Innovations for Sustainable Development (pp. 55–96). Springer.

- Vilgelm, A. E., & Richmond, A. (2019). Chemokines modulate immune surveillance in tumorigenesis, metastasis, and response to immunotherapy. Frontiers in immunology, 10, 333.

- Wen, X. (2020). Shape Control Synthesis and Microstructure Studies of Metal Nanoparticles Chalmers Tekniska Hogskola (Sweden)].

- Xi, Y., Akram, S., Yang, X., Hu, B., Saddique, M. A. B., Guan, G., Tian, D., Luo, X., & Ren, M. (2025). Innovative Strategies for Plant Protection: The Combination of Spray-Induced Gene Silencing and Nanotechnology. Journal of Agricultural and Food Chemistry.

- Xiao, Y., Ahmad, T., Belwal, T., Aadil, R. M., Siddique, M., Pang, L., & Xu, Y. (2023). A review on protein based nanocarriers for polyphenols: Interaction and stabilization mechanisms. Food Innovation and Advances, 2(3), 193–202.

- Yasmin, A., Khatun, F., Rahman, S. A., Anik, Z. H., & Hasan, M. (2024). Infectious and Non-Infectious Diseases of Farm Animals in Natore District of Bangladesh. Research in Agriculture Livestock and Fisheries, 11(3), 327–341.

- Yassin, M. T., Al-Askar, A. A., Maniah, K., & Al-Otibi, F. O. (2022). Green synthesis of zinc oxide nanocrystals utilizing Origanum majorana leaf extract and their synergistic patterns with colistin against multidrug-resistant bacterial strains. Crystals, 12(11), 1513.

- Zamani, A., Marjani, A. P., & Mousavi, Z. (2019). Agricultural waste biomass-assisted nanostructures: Synthesis and application. Green Processing and Synthesis, 8(1), 421–429.

- Zhang, D., Gokce, B., & Barcikowski, S. (2017). Laser synthesis and processing of colloids: fundamentals and applications. Chemical reviews, 117(5), 3990–4103.

- Zhang, R., Khalizov, A., Wang, L., Hu, M., & Xu, W. (2012). Nucleation and growth of nanoparticles in the atmosphere. Chemical reviews, 112(3), 1957–2011.

- Zhang, X., Li, G., Wu, D., Liu, J., & Wu, Y. (2020). Recent advances on emerging nanomaterials for controlling the mycotoxin contamination: From detection to elimination. Food Frontiers, 1(4), 360–381.

- Zulfiqar, N., Nadeem, R., & Musaimi, O. A. (2024). Photocatalytic degradation of antibiotics via exploitation of a magnetic nanocomposite: a green nanotechnology approach toward drug-contaminated wastewater reclamation. ACS omega, 9(7), 7986–8004.