| Journal Name: | Journal of Engineering Research and Reports |
| --- | --- |
| Manuscript Number: | Ms_JERR_155734 |
| Title of the Manuscript: | The Effect of Thermal Cycling Cycles on the Microstructure and Properties of Cu/In-48Sn-xGNSs/Cu Solder Joints |
| Type of the Article | Research Article |

PART 1(Importance of the manuscript)

|  | Comments of the Reviewers | Author’s Feedback |
| --- | --- | --- |
| Please write a few sentences regarding the importance of this manuscript for the scientific community. A minimum of 3-4 sentences may be required for this part. | The manuscript provides a systematic and well-structured study on the effect of thermal cycling on composite solder joints. The experimental findings are consistent and provide valuable insights into microstructural stability and fracture study. However few minor issues are should be addressed before publication - Provide a quantitative correlation between shear strength degradation and IMC thickness - Fracture mechanics needs supporting evidence - Improve minor language and formatting for better readability | 1. As the number of thermal cycles increased from 200 to 1,000, the IMC layer thickness at both joints continued to increase, while the shear strength decreased in tandem, showing a significant linear negative correlation between the two. The fits between shear strength and IMC thickness for the In-48Sn and In-48Sn-0.05GNSs joints are shown below: σ=-3.32×d+20.8 In the equation：σ——Shear strength d——IMC thickness Slope: a = -3.32 MPa/μm；Intercept b = 20.8 MPa；Coefficient of determination R2 = 0.981. σ=-1.96×d+22.9 Slope: a = -1.96 MPa/μm；Intercept b = 22.9 MPa；Coefficient of determination R2 = 0.984. For every 1 μm increase in IMC thickness, the shear strength of In-48Sn joints decreases by an average of approximately 3.32 MPa. In contrast, the shear strength of In-48Sn-0.05GNSs joints decreases by an average of approximately 1.96 MPa, representing a rate of decline that is only 59% of that observed in joints without graphene. This indicates that graphene significantly mitigates the adverse effects of IMC growth on shear strength. 2. After 600 thermal cycles of In-48Sn composite solder joints, ductile pits can still be observed in Figures (c) and (d). In the upper left corner of Figure (c), localized flaking-like brittle fracture surfaces and the appearance of the Cu₂(In,Sn) phase can be observed. This indicates that an increase in the number of thermal cycles leads to a thickening of the IMC layer and an intensification of interfacial stress concentration. The fracture zone shifts from the in-situ reaction zone to the interfacial reaction zone, resulting in a decrease in plastic deformation capacity. At this stage, the fracture transitions from ductile to brittle fracture. Based on relevant studies and the aforementioned characteristics, the fracture mechanism is identified as typical mixed fracture. After 1,000 thermal cycles, the fracture mechanism of the In-48Sn composite solder joints is brittle fracture. Figures (e–f) show that the fracture surface is noticeably flattened, with no obvious tearing marks, and localized detachment along the IMC layer, indicating that tensile fracture is primarily due to brittle fracture of the IMC layer. After 200 thermal cycles, the joints made with the In-48Sn-0.05GNSs composite solder alloy exhibited typical high-toughness fracture. As shown in Figures (g–h), the fracture surface appears relatively smooth, with deep and uniform ductile dimples and uniformly distributed local voids, indicating good crack resistance—a typical characteristic of high-toughness fracture. 3. The formatting and language have been corrected and made more appropriate. |

PART  2.1 (Objective Evaluation)

|  | Rating of the Reviewers | Author’s Feedback |
| --- | --- | --- |
| 1. Is the title clear and appropriate for the study? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 3 | Thanks for the evaluation and rating |
| 2. Is the abstract of the article comprehensive? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 4 | Thanks for the evaluation and rating |
| 3. Are the keywords appropriate and useful? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 3 | Thanks for the evaluation and rating |
| 4. Is the background information of the paper sufficient and well organized? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 3 | Thanks for the evaluation and rating |
| 5. Are the research objectives/hypotheses clearly stated? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 4 | Thanks for the evaluation and rating |
| 6. Is the literature review relevant and up to date? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 4 | Thanks for the evaluation and rating |
| 7. Is the research methodology appropriate for the study? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 3 | Thanks for the evaluation and rating |
| 8. Were ethical issues properly addressed (if applicable)? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 3 | Thanks for the evaluation and rating |
| 9. Are the results presented clearly? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 4 | Thanks for the evaluation and rating |
| 10. Are tables and figures clear, relevant, and necessary? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 3 | Thanks for the evaluation and rating |
| 11. Does the discussion relate findings to existing literature? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 4 | Thanks for the evaluation and rating |
| 12. Are the conclusions supported by the data? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 3 | Thanks for the evaluation and rating |
| 13. Are the limitations of the study discussed? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable |  | Thanks for the evaluation and rating |
| 14. Are the references relevant and sufficient (in number)? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 4 | Thanks for the evaluation and rating |
| 15. Is the manuscript written in clear and understandable language? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 3 | Thanks for the evaluation and rating |

PART  2.2 (Subjective Evaluation)

|  | Reviewer’s comment | Author’s Feedback (It is mandatory that authors should write his/her feedback here) |
| --- | --- | --- |
| Is the title of the article suitable? If your answer is NO, please provide a brief, clear suggestion for improvement. | yes | Thanks for the evaluation and rating |
| Is the abstract of the article comprehensive? If your answer is NO, please provide a brief, clear suggestion for improvement. | yes | Thanks for the evaluation and rating |
| Is the manuscript scientifically correct? If your answer is NO, please provide a brief, clear suggestion for improvement. | yes | Thanks for the evaluation and rating |
| Are the references sufficient and recent? (YES or NO) If your answer is NO, please provide clear suggestion for improvement. | yes | Thanks for the evaluation and rating |

| Editorial Comments (This section is reserved for the comments from journal editorial office and editors): |  |
| --- | --- |
|  | Author’s Feedback |
| The manuscript presents a systematic study on the effect of thermal cycling in composite solder joints. The findings are generally consistent and provide valuable insights into fracture behaviour and microstructural stability. However the study require minor revision - Correlation between fracture behaviour and microstructure stability - Detailed Fracture mechanics and supporting evidence - Minor language correction Few minor issues are should be addressed before publication 1. Provide a quantitative correlation between shear strength degradation and IMC thickness 2. Fracture mechanics needs supporting evidence Improve minor language and formatting for better readability | 1. We supplemented the correlation between fracture behaviour and microstructure stability, clarifying how grain coarsening and interfacial IMC growth dominate the transition of fracture modes during thermal cycling. 2. Detailed fracture mechanics evidence was added, including the analysis of ductile/brittle fracture characteristics, crack propagation resistance, and plastic energy dissipation mechanism, which provides solid support for the fracture mechanism discussion. 3. All minor language errors were corrected, and the overall formatting (figure numbering, unit specification, symbol standardization, etc.) was uniformly optimized to greatly improve the readability of the manuscript. 4. A quantitative linear correlation between shear strength degradation and IMC thickness was established with fitting equations and correlation coefficients, which quantifies the influence of IMC growth on shear property degradation. All revisions have been carefully checked and completed, and we believe the revised manuscript meets the publication requirements of the journal. We sincerely appreciate your review and guidance. |

| PART 3: |  |  |
| --- | --- | --- |
|  | ## Reviewer’s comment | Author’s Feedback (It is mandatory that authors should write his/her feedback here) |
| Are there ethical issues in this manuscript? | (If yes, Kindly please write down the ethical issues here in details) | There are no ethical issues involved in this manuscript. The study only involves material preparation, microstructure characterization, and property testing of solder joints, without involving human subjects, animal experiments, biological samples, data falsification, plagiarism, or any other unethical research behaviors. All experimental operations and data processing comply with academic norms and relevant research standards. |