| Journal Name: | Journal of Engineering Research and Reports |
| --- | --- |
| Manuscript Number: | Ms_JERR_155734 |
| Title of the Manuscript: | The Effect of Thermal Cycling Cycles on the Microstructure and Properties of Cu/In-48Sn-xGNSs/Cu Solder Joints |
| Type of the Article | Research Article |

PART 1(Importance of the manuscript)

|  | Comments of the Reviewers | Author’s Feedback |
| --- | --- | --- |
| Please write a few sentences regarding the importance of this manuscript for the scientific community. A minimum of 3-4 sentences may be required for this part. | Limited research on the effects of thermal cycling cycles on the microstructure and properties of In-48Sn brazing alloys. Your work primarily is to investigate the effects of thermal cycling cycles on the microstructure, shear properties, and shear fracture morphology of the solder joints. | This work systematically investigates the microstructure evolution, interfacial IMC growth, and shear property degradation of low-melting In-48Sn-xGNSs solder joints under thermal cycling, filling the research gap of thermal fatigue reliability for low-temperature In-based composite solders. A quantitative linear correlation between shear strength degradation and IMC thickness is established, which provides a measurable basis for reliability evaluation and life prediction of low-temperature electronic packaging solder joints. The addition of a small amount of graphene nanosheets effectively suppresses grain coarsening and IMC thickening, slows down strength loss, and maintains better fracture toughness, offering a feasible strategy for developing high-reliability low-temperature lead-free solders for electronic packaging. |

PART  2.1 (Objective Evaluation)

|  | Rating of the Reviewers | Author’s Feedback |
| --- | --- | --- |
| 1. Is the title clear and appropriate for the study? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 4 | Thanks for the evaluation and rating |
| 2. Is the abstract of the article comprehensive? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 3 | Thanks for the evaluation and rating |
| 3. Are the keywords appropriate and useful? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 4 | Thanks for the evaluation and rating |
| 4. Is the background information of the paper sufficient and well organized? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 3 | Thanks for the evaluation and rating |
| 5. Are the research objectives/hypotheses clearly stated? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 4 | Thanks for the evaluation and rating |
| 6. Is the literature review relevant and up to date? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 3 | Thanks for the evaluation and rating |
| 7. Is the research methodology appropriate for the study? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 4 | Thanks for the evaluation and rating |
| 8. Were ethical issues properly addressed (if applicable)? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 5 | Thanks for the evaluation and rating |
| 9. Are the results presented clearly? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 4 | Thanks for the evaluation and rating |
| 10. Are tables and figures clear, relevant, and necessary? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 4 | Thanks for the evaluation and rating |
| 11. Does the discussion relate findings to existing literature? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 4 | Thanks for the evaluation and rating |
| 12. Are the conclusions supported by the data? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 4 | Thanks for the evaluation and rating |
| 13. Are the limitations of the study discussed? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 4 | Thanks for the evaluation and rating |
| 14. Are the references relevant and sufficient (in number)? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 3 | Thanks for the evaluation and rating |
| 15. Is the manuscript written in clear and understandable language? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 4 | Thanks for the evaluation and rating |

PART  2.2 (Subjective Evaluation)

|  | Reviewer’s comment | Author’s Feedback (It is mandatory that authors should write his/her feedback here) |
| --- | --- | --- |
| Is the title of the article suitable? If your answer is NO, please provide a brief, clear suggestion for improvement. | YES | Thanks for the evaluation and rating |
| Is the abstract of the article comprehensive? If your answer is NO, please provide a brief, clear suggestion for improvement. | NO The abstract written in the submitted manuscript needs some quantitative findings. | During thermal cycling, the grain size of the γ-InSn₄ phase in the In-48Sn solder joints increased from 10.4 μm to 28.6 μm, the IMC thickness increased from 3.639 μm to 5.462 μm, and the shear strength decreased from 7.9 MPa to 3.1 MPa; After adding 0.05 wt.% graphene, the grain size of the γ-InSn₄ phase increased only from 4.1 μm to 13.8 μm, the IMC thickness increased from 3.174 μm to 4.915 μm, and the shear strength decreased from 16.9 MPa to 12.7 MPa. It was concluded that, under the same thermal cycling conditions, both the grain coarsening rate and the intermetallic compound (IMC) growth rate of the In-48Sn-0.05GNS composite brazing joints were significantly lower than those of the In-48Sn joints, while still maintaining high shear strength. |
| Is the manuscript scientifically correct? If your answer is NO, please provide a brief, clear suggestion for improvement. | NO Provide a clear justification on Thermal cycling parameters used in your research studies. Growth mechanism explanations can be highlighted precisely. In your research manuscript conclusion section is very descriptive, arrange accordingly the findings and precisely update your findings. | The melting point of the In-48Sn brazing alloy is approximately 118°C. To ensure that the solder joints do not melt, the temperature range for the thermal cycling test was set to -35°C to 110°C, with a holding time of 15 minutes for both the high-temperature and low-temperature phases, and a heating and cooling rate of 10°C/min. The number of thermal cycles was set to 200, 400, 600, 800, and 1,000, respectively, with each thermal cycle lasting approximately 45 minutes. The growth mechanism of IMC controlled by atomic diffusion and the Zener pinning effect of graphene has been precisely emphasized. The conclusion section has been reorganized to highlight core findings with quantitative data for better preciseness. |
| Are the references sufficient and recent? (YES or NO) If your answer is NO, please provide clear suggestion for improvement. | YES | Thanks for the evaluation and rating |

| PART 3: |  |  |
| --- | --- | --- |
|  | ## Reviewer’s comment | Author’s Feedback (It is mandatory that authors should write his/her feedback here) |
| Are there ethical issues in this manuscript? | (If yes, Kindly please write down the ethical issues here in details) | There are no ethical issues involved in this manuscript. The study only involves material preparation, microstructure characterization, and property testing of solder joints, without involving human subjects, animal experiments, biological samples, data falsification, plagiarism, or any other unethical research behaviors. All experimental operations and data processing comply with academic norms and relevant research standards. |